Supporting information

Room-temperature martensitic actuation profited from one-dimensional hybrid perovskite structure

Bei-Dou Liang, Chang-Chun Fan, Cheng-Dong Liu, Chao-Yang Chai, Xiang-Bin Han* and Wen Zhang*

Jiangsu Key Laboratory for Science and Applications of Molecular Ferroelectrics and School of Chemistry and Chemical Engineering, Southeast University, Nanjing 211189, China.

E-mail: hanxiangbin@seu.edu.cn; zhangwen@seu.edu.cn

Experimental

Table S1. Crystallographic data and structure refinement details for 1 at different phases.

Table S2. Pb-I bond lengths of 1 in LTP, ITP, and HTP.

Table S3. Converted cell parameters for spontaneous strain calculation.

Fig. S1. Experimental and simulated PXRD patterns for powder sample of 1 at HTP.

Fig. S2. TGA measurement of 1. The decomposition begins at about 500 K.

Fig. S3. Single crystal orientation.

Fig. S4. Dielectric constant curves of 1 at different frequencies.

Fig. S5. Hirshfeld surfaces for 1 of [PbI3]n.

Fig. S6. Order-disorder change of cations during the phase transitions. The NMEA cation in thermal ellipsoid mode with 50% probability.

Fig. S7. Phase boundary moving observed from (100) when crystals transition from the HTP to ITP.

Experimental

Materials and general characterizations

Reagents used were in analytical grade without further purification. Powder X-ray diffraction (PXRD) patterns were obtained on a Rigaku SmartLab X-ray diffractometer at room temperature. The diffraction patterns were collected in the 2θ range of 5−50° with a step size of 0.02°. DSC measurements were performed on a NETZSCH DSC 200F3 instrument under N2 at atmospheric pressure with a heating/cooling rate of 20 K min−1. Ultraviolet-vis (UV-vis) absorption spectra were measured with Shimadzu UV-2600 equipped with ISR-2600Plus integrating sphere.

Single-crystal X-ray Diffraction

Crystallographic data of the salts were collected on a Rigaku Oxford Diffraction Supernova Dual Source, Cu at Zero equipped with an AtlasS2 CCD using Mo Kα radiation and an XtaLAB Synergy R, DW system, HyPix diffractometer. SHELXL-2018 software package was used to solve the structures by direct methods. All non-hydrogen atoms were refined anisotropically. The positions of hydrogen atoms were generated geometrically.

Dielectric spectra

Temperature-dependent dielectric constant spectra were measured on powdered samples by using a Tonghui TH2828A impedance analyzer at frequencies of 1−1000 kHz with an applied electric field of 1 V.

Table S1. Crystallographic data and structure refinement details for 1 at different phases.

|  | LTP-173K | ITP-253K | HTP-333K |
| --- | --- | --- | --- |
| Formula | C6H20N2I6Pb2 | C3H10NI3Pb | C3H10NI3Pb |
| Formula weight | 1296.04 | 648.02 | 648.02 |
| Crystal system | Triclinic | Monoclinic | Hexagonal |
| space group | P-1 | C2/c | P63/mmc |
| a / Å | 8.1501(3) | 9.8984(9) | 9.2432(5) |
| b / Å | 9.0775(2) | 15.0923(10) | 9.2432(5) |
| c / Å | 15.8322(3) | 8.0597(5) | 8.1797(4) |
| α / ° | 83.8690(10) | 90 | 90 |
| β / ° | 84.399(2) | 97.887(7) | 90 |
| γ / ° | 87.646(2) | 90 | 120 |
| V / Å3 | 1158.49(5) | 1192.65(15) | 605.22(7) |
| Z | 2 | 4 | 2 |
| Dcalc / g·cm−3 | 3.715 | 3.609 | 3.501 |
| μ / mm−1 | 22.495 | 21.851 | 21.527 |
| Reflns. collected | 28600 | 6472 | 6429 |
| Obsd. reflns. [I>2σ(I)] | 5081 | 1133 | 202 |
| Rint | 0.0493 | 0.0432 | 0.0777 |
| R1a/wR2b [I>2σ(I)] | 0.0599,0.1654 | 0.0516,0.1512 | 0.0577,0.1694 |
| R1/wR2 (all data) | 0.0679,0.1678 | 0.0690,0.1591 | 0.0931,0.1950 |
| GOF | 1.186 | 1.103 | 1.035 |
| Δρc / eÅ–3 | 3.247/-3.304 | 2.606/-0.996 | 0.654/-0.995 |

a R1 = Σ||Fo| – |Fc||/Σ|Fo|. b wR2(F2) = [Σw(Fo2 – Fc2)2/ΣwFo4]1/2. c Maximum and minimum residual electron density.

Table S2. Pb-I bond lengths of 1 in LTP, ITP, and HTP.

| Bond lengths | Length / Å |
| --- | --- |
| LTP-173K |  |
| I(5)Pb(1) | 3.4007(10) |
| I(6)Pb(1)ii | 3.3409(11) |
| I(3)Pb(2) | 3.3741(10) |
| I(1)Pb(2)i | 3.3100(11) |
| I(2)Pb(2)i | 3.2564(11) |
| I(2)Pb(1) | 3.2355(11) |
| I(4)Pb(2) | 3.2192(10) |
| I(4)Pb(1) | 3.2143(11) |
| I(5)Pb(2) | 3.1664(10) |
| I(3)Pb(1) | 3.1235(10) |
| I(1)Pb(1) | 3.1036(10) |
| I(6)Pb(2) | 3.0992(10) |
| Symmetry codes: (i) 1+x, +y, +z; (ii) 1+x, +y, +z. |  |
| ITP-253K |  |
| I(2)Pb(1)i | 3.2394(12) |
| I(2)Pb(1) | 3.2227(10) |
| I(1)Pb(1) | 3.2047(10) |
| I(1)Pb(1)i | 3.2047(10) |
| Symmetry codes: (i) 1x, +y, 3/2z. |  |
| HTP-333K |  |
| I(1)Pb(1) | 3.2249(19) |
| I(1)Pb(1)i | 3.2249(19) |
| Symmetry codes: (i) x, y, 1/2+z. |  |

Table S3. Converted cell parameters for spontaneous strain calculation.

|  | LTP-ITP Transition | ITP-HTP Transition |
| --- | --- | --- |
| a / Å | 9.0775(2) | 9.8984(9) |
| b / Å | 15.8322(3) | 15.0923(10) |
| c / Å | 8.1501(3) | 8.0597(5) |
| α / ° | 95.601(2) | 90 |
| β / ° | 87.646(2) | 97.887(7) |
| γ / ° | 96.310(10) | 90 |
| a0 / Å | 9.8984(9) | 9.2432(5) |
| b0 / Å | 15.0923(10) | 16.0097(9) |
| c0 / Å | 8.0597(5) | 8.1797(4) |
| α0 / ° | 90 | 90 |
| β0 / ° | 97.887(7) | 90 |
| γ0 / ° | 90 | 90 |

Fig. S1. Experimental and simulated PXRD patterns for powder sample of 1 at HTP.

Fig. S2. TGA measurement of 1. The decomposition begins at about 500 K.

Fig. S3. Single crystal orientation.

Fig. S4. Dielectric constant curves of 1 at different frequencies.

Fig. S5. Hirshfeld surfaces for 1 of [PbI3]n.

Fig. S6. Order-disorder change of cations during the phase transitions. The NMEA cation in thermal ellipsoid mode with 50% probability.

Fig. S7. Phase boundary moving observed from (100) when crystals transition from the HTP to ITP.