Improving the performance of DSSCs by modulating the electron donor and electron acceptor of dye molecules with the DTPBT group as π-bridge

Shihan Zhaoa, Qian Liua*, and Jiameng Caoa

aXi'an University of Technology, Xi'an, China

Shihan Zhao (zhaoshihan@stu.xaut.edu.cn), Qian Liu(1135099487@qq.com), Jiameng Cao (cjm@stu.xaut.edu.cn)

Table S1. Experimental parameters of H1 molecule.

| Dye | λmax/nm | Jsc/mA cm-2 | Voc/V | FF | PCE (%) | Γ |
| --- | --- | --- | --- | --- | --- | --- |
| H1 | 476 | 8.41 | 0.692 | 0.71 | 4.13 | 1.26×10-7 |

Table S2. The parameters related to the performance of dye molecules H1, Q1, and Q2.

- Edye* is the excited state oxidation potential of the dye.

- ∆Ginject is the free energy of electron injection.

- μnormal is the vertical dipole moment of the dye molecule.

- LHE is light capture efficiency.

- τ is the excited state lifetime of the dye molecule.

| Dyes | Edye* a | ∆Ginject b | μnormal c | LHE d | τ/ns e | ∆Gregen |
| --- | --- | --- | --- | --- | --- | --- |
| H1 | 2.1242 | -1.8758 | 12.6076 | 0.976 | 1.83 | 0.107 |
| Q1 | 2.201 | -1.799 | 16.7531 | 0.992 | 1.43 | 0.184 |
| Q2 | 2.6425 | -1.3575 | 16.5241 | 0.995 | 1.64 | 0.320 |

Table S3. Calculate the relevant parameters of PCE for DSSCs.

| Dye | volum /Bohr3 | Γ/ (10-7mol cm-2) | ΔECB | nc/ (1020 cm-3) |
| --- | --- | --- | --- | --- |
| H1 | 7652.62 | 1.26 | 0.05 | 0.02564 |
| Q1 | 8876.28 | 1.08 | 0.05 | 0.02073 |
| Q2 | 9087.98 | 1.06 | 0.09 | 0.00484 |

H1

(a)

Q1

(b)

Q2

(c)

Figure S1. The optimized configuration of dye molecules.

H1-TiO2

Q1-TiO2

(a)

Q2-TiO2

(b)

(c)

Figure S2. The optimized configuration of dyes/TiO2.

(a)

(b)

Figure S3. The PDOS graph of dyes/TiO2.