# Supporting information

Preparation of bimetal modified HMS zeolite and its catalytic effect on phenol degradation

Yaming Pang a,b, Liguo Gao a,b,*, Mingxuan Xia a,c , Yuxiu Fu a,b, Xiaoli, Song a,b

a School of Chemistry and Chemical Engineering, Yulin University, Yulin, 719000, Shaanxi, China

b Shaanxi Key Laboratory of Low Metamorphic Coal Clean Utilization, Yulin, 719000, Shaanxi, China

c College of Oil and Gas Engineering, Southwest Petroleum University, Chengdu, 610500,Szechwan, China

Figure S1. FTIR spectrum of (A)HMS、(B)Ti-HMS、(C)Ce-HMS、(D)Ce/Ti-HMS

Table S1

Box-BehnKen experimental design and results display

| NO | Time（min） | Temperature（℃） | Amount of catalyst（g/mL） | Phenol removal rate（%） |
| --- | --- | --- | --- | --- |
| 1 2 3 4 5 6 7 8 9 10 11 12 13 14 15 16 17 | 210 60 180 180 180 210 60 210 60 210 180 180 180 180 120 60 210 | 60 20 60 20 40 40 40 20 40 40 60 60 60 60 20 60 40 | 0.10 0.10 0.05 0.05 0.10 0.10 0.15 0.10 0.05 0.05 0.10 0.15 0.10 0.15 0.10 0.10 0.15 | 89.9 48.7 72.6 46.6 77.8 78.3 70.4 53.5 52.2 54.7 84.7 83.9 84.7 78.6 60.7 60.6 80.1 |

Table S2

Significance test of regression equation coefficient

| No | Sum of square | Degree of freedom | Mean square | F | P |
| --- | --- | --- | --- | --- | --- |
| Model | 3150.93 | 9 | 345.10 | 24.54 | 0.0002 |
| A-Time | 270.73 | 1 | 270.73 | 19.25 | 0.0032 |
| B-Temperature | 558.05 | 1 | 549.97 | 39.10 | 0.0004 |
| C-Agent oil ratio | 549.97 | 1 | 558.05 | 39.68 | 0.0004 |
| AB | 0.74 | 1 | 0.74 | 0.035 | 0.0825 |
| AC | 52.23 | 1 | 52.23 | 3.71 | 0.0095 |
| BC | 40.14 | 1 | 40.14 | 2.85 | 0.0135 |
| A² | 154.67 | 1 | 154.67 | 11.00 | 0.0128 |
| B² | 102.26 | 1 | 102.26 | 7.27 | 0.0308 |
| C² | 149.90 | 1 | 149.90 | 10.66 | 0.0138 |
| Residual | 98.46 | 7 | 14.07 |  |  |
| Lack of fit | 84.41 | 5 | 16.88 |  |  |
| Pure error | 14.05 | 2 | 7.02 |  |  |
| Sum | 3204.39 | 16 |  |  |  |

Figure S2. Contour line and response surface of the effect of reaction time and catalyst dosage on Phenol removal rate

Figure S3. Contour line and response surface of the effect of reaction time and reaction temperature on Phenol removal rate

Figure S4. Contour line and response surface of the effect of catalyst dosage and reaction temperature on Phenol removal rate

Fig.S5 Infrared spectra of phenol solution before and after degradation

Figure S6 Determination of hydroxyl radicals

| Atom | X/Y/Z coordinate(Angstrom) |  |  |
| --- | --- | --- | --- |
| Si | 0.169822 | 0.356758 | 0.399061 |
| Si | 0.200672 | 0.392497 | 0.894388 |
| Si | 0.367035 | 0.316598 | 0.596196 |
| Si | 0.133102 | 0.159404 | 0.586121 |
| Si | 0.290818 | 0.106068 | 0.890280 |
| Si | 0.108479 | 0.211369 | 0.078918 |
| Si | 0.340049 | 0.103171 | 0.421491 |
| Si | 0.797890 | 0.395234 | 0.406375 |
| Si | 0.842740 | 0.375001 | 0.891816 |
| Si | 0.894434 | 0.210702 | 0.579142 |
| Si | 0.612032 | 0.294940 | 0.585854 |
| Si | 0.870309 | 0.176296 | 0.082201 |
| Si | 0.666204 | 0.146470 | 0.900972 |
| Si | 0.644658 | 0.360702 | 0.087994 |
| Si | 0.712445 | 0.114979 | 0.391542 |
| Si | 0.283766 | 0.873598 | 0.425578 |
| Si | 0.321246 | 0.862765 | 0.910697 |
| Si | 0.387000 | 0.696212 | 0.603384 |
| Si | 0.103513 | 0.784935 | 0.605162 |
| Si | 0.364147 | 0.665892 | 0.099072 |
| Si | 0.164924 | 0.630242 | 0.908575 |
| Si | 0.127243 | 0.829847 | 0.112495 |
| Si | 0.213729 | 0.600961 | 0.411409 |
| Si | 0.665637 | 0.873217 | 0.408881 |
| Si | 0.704658 | 0.899895 | 0.918915 |
| Si | 0.863272 | 0.834321 | 0.604707 |
| Si | 0.632182 | 0.676125 | 0.597914 |
| Si | 0.886381 | 0.793304 | 0.103745 |
| Si | 0.793024 | 0.617370 | 0.902552 |
| Si | 0.606378 | 0.717860 | 0.094283 |
| Si | 0.832907 | 0.634870 | 0.407519 |
| Ce | 0.405484 | 0.289993 | 0.130218 |
| O | 0.287808 | 0.376489 | 0.736226 |
| O | 0.379020 | 0.180775 | 0.580065 |
| O | 0.273719 | 0.399566 | 0.060533 |
| O | 0.360970 | 0.988180 | 0.886944 |
| O | 0.380212 | 0.203732 | 0.898431 |
| O | 0.403374 | 0.140973 | 0.258825 |
| O | 0.202248 | 0.111695 | 0.422033 |
| O | 0.125634 | 0.295902 | 0.564676 |
| O | 0.111641 | 0.292404 | 0.917972 |
| O | 0.118239 | 0.291293 | 0.243141 |
| O | 0.197197 | 0.111109 | 0.744671 |
| O | 0.999487 | 0.133396 | 0.089147 |
| O | 0.369375 | 0.973469 | 0.444509 |
| O | 0.309715 | 0.345984 | 0.411235 |
| O | 0.215865 | 0.125539 | 0.062658 |
| O | 0.003219 | 0.127909 | 0.588568 |
| O | 0.887365 | 0.300250 | 0.734129 |
| O | 0.793399 | 0.123445 | 0.554116 |
| O | 0.885607 | 0.311385 | 0.058185 |
| O | 0.632392 | 0.017148 | 0.911070 |
| O | 0.802756 | 0.138398 | 0.915597 |
| O | 0.794196 | 0.128323 | 0.230996 |
| O | 0.620093 | 0.218005 | 0.414290 |
| O | 0.709344 | 0.386579 | 0.564152 |
| O | 0.706475 | 0.385834 | 0.913052 |
| O | 0.723309 | 0.389508 | 0.242213 |
| O | 0.623167 | 0.208902 | 0.737679 |
| O | 0.524333 | 0.417414 | 0.116412 |
| O | 0.636702 | 0.004993 | 0.387725 |
| O | 0.888779 | 0.291229 | 0.417685 |
| O | 0.616356 | 0.224234 | 0.060416 |
| O | 0.492564 | 0.362595 | 0.599709 |
| O | 0.370387 | 0.784276 | 0.758262 |
| O | 0.293224 | 0.600841 | 0.577241 |
| O | 0.363427 | 0.802744 | 0.080295 |
| O | 0.123768 | 0.505249 | 0.874380 |
| O | 0.301378 | 0.619064 | 0.931858 |
| O | 0.296808 | 0.611434 | 0.251677 |
| O | 0.118209 | 0.700770 | 0.440251 |
| O | 0.202464 | 0.873704 | 0.589593 |
| O | 0.185514 | 0.877039 | 0.944625 |
| O | 0.197819 | 0.874561 | 0.270370 |
| O | 0.116494 | 0.705090 | 0.761107 |
| O | 0.996434 | 0.867140 | 0.128332 |
| O | 0.142457 | 0.488434 | 0.398581 |
| O | 0.373237 | 0.768597 | 0.435086 |
| O | 0.122020 | 0.693544 | 0.082084 |
| O | 0.992616 | 0.866279 | 0.616237 |
| O | 0.789203 | 0.885415 | 0.759501 |
| O | 0.875568 | 0.698110 | 0.576424 |
| O | 0.785749 | 0.888175 | 0.082037 |
| O | 0.873018 | 0.505232 | 0.884145 |
| O | 0.882793 | 0.716122 | 0.931928 |
| O | 0.876660 | 0.702697 | 0.250288 |
| O | 0.696604 | 0.629349 | 0.428330 |
| O | 0.618520 | 0.812418 | 0.575262 |
| O | 0.611955 | 0.803295 | 0.937276 |
| O | 0.617376 | 0.800468 | 0.255877 |
| O | 0.706699 | 0.631820 | 0.750178 |
| O | 0.497447 | 0.641913 | 0.103970 |
| O | 0.873447 | 0.505011 | 0.405210 |
| O | 0.801789 | 0.876199 | 0.436063 |
| O | 0.709129 | 0.625321 | 0.065872 |
| O | 0.507047 | 0.631437 | 0.613139 |

| Atom | X/Y/Z coordinate(Angstrom) |  |  |
| --- | --- | --- | --- |
| Si | 0.165966 | 0.362628 | 0.400137 |
| Si | 0.200482 | 0.390620 | 0.899789 |
| Si | 0.366590 | 0.325270 | 0.593797 |
| Si | 0.133744 | 0.164585 | 0.590060 |
| Si | 0.295310 | 0.108627 | 0.894741 |
| Si | 0.108283 | 0.209726 | 0.086241 |
| Si | 0.340400 | 0.118819 | 0.410167 |
| Si | 0.793979 | 0.393057 | 0.407246 |
| Si | 0.836102 | 0.369671 | 0.899251 |
| Si | 0.891543 | 0.205826 | 0.586756 |
| Si | 0.611293 | 0.297163 | 0.592141 |
| Si | 0.868886 | 0.167867 | 0.089276 |
| Si | 0.665952 | 0.139968 | 0.902823 |
| Si | 0.635959 | 0.348592 | 0.095616 |
| Si | 0.710390 | 0.111407 | 0.399662 |
| Si | 0.288576 | 0.882891 | 0.413811 |
| Si | 0.327042 | 0.864631 | 0.906786 |
| Si | 0.388479 | 0.698321 | 0.597534 |
| Si | 0.108277 | 0.792817 | 0.600622 |
| Si | 0.366737 | 0.663128 | 0.096993 |
| Si | 0.167733 | 0.632514 | 0.905353 |
| Si | 0.129315 | 0.835679 | 0.104462 |
| Si | 0.210703 | 0.604644 | 0.407746 |
| Si | 0.663056 | 0.870478 | 0.408906 |
| Si | 0.702685 | 0.894385 | 0.913649 |
| Si | 0.865138 | 0.832795 | 0.601709 |
| Si | 0.633435 | 0.671828 | 0.598514 |
| Si | 0.888746 | 0.792325 | 0.099409 |
| Si | 0.795968 | 0.613547 | 0.904240 |
| Si | 0.607668 | 0.712982 | 0.096057 |
| Si | 0.836892 | 0.632913 | 0.405177 |
| Ti | 0.397851 | 0.290615 | 0.101143 |
| O | 0.288665 | 0.375914 | 0.744421 |
| O | 0.381879 | 0.187187 | 0.576169 |
| O | 0.276903 | 0.387507 | 0.067728 |
| O | 0.369367 | 0.991473 | 0.887299 |
| O | 0.388659 | 0.207260 | 0.907011 |
| O | 0.396531 | 0.178259 | 0.253444 |
| O | 0.201588 | 0.119620 | 0.422745 |
| O | 0.121051 | 0.302313 | 0.568457 |
| O | 0.108877 | 0.291397 | 0.923296 |
| O | 0.114271 | 0.293024 | 0.246952 |
| O | 0.204447 | 0.117639 | 0.745668 |
| O | 0.000582 | 0.128360 | 0.097353 |
| O | 0.373985 | 0.986216 | 0.409293 |
| O | 0.305276 | 0.360788 | 0.417889 |
| O | 0.217652 | 0.123598 | 0.064409 |
| O | 0.004764 | 0.126417 | 0.597576 |
| O | 0.881075 | 0.294135 | 0.742536 |
| O | 0.792303 | 0.114552 | 0.563000 |
| O | 0.878420 | 0.305210 | 0.066862 |
| O | 0.627360 | 0.010574 | 0.901489 |
| O | 0.803809 | 0.126399 | 0.921771 |
| O | 0.794596 | 0.119852 | 0.240339 |
| O | 0.620723 | 0.217930 | 0.423376 |
| O | 0.709751 | 0.389888 | 0.571311 |
| O | 0.698547 | 0.384893 | 0.924049 |
| O | 0.710638 | 0.388553 | 0.250058 |
| O | 0.623036 | 0.209754 | 0.744323 |
| O | 0.507878 | 0.396082 | 0.114721 |
| O | 0.630261 | 0.003051 | 0.392120 |
| O | 0.883716 | 0.286324 | 0.423307 |
| O | 0.618444 | 0.211024 | 0.067926 |
| O | 0.493388 | 0.369808 | 0.605803 |
| O | 0.373033 | 0.786400 | 0.752865 |
| O | 0.292089 | 0.603778 | 0.572461 |
| O | 0.368733 | 0.801238 | 0.075354 |
| O | 0.124347 | 0.505846 | 0.884803 |
| O | 0.305417 | 0.616121 | 0.928706 |
| O | 0.296186 | 0.612517 | 0.249911 |
| O | 0.119242 | 0.709805 | 0.434861 |
| O | 0.207414 | 0.884157 | 0.580154 |
| O | 0.189781 | 0.882303 | 0.936521 |
| O | 0.200054 | 0.881413 | 0.261039 |
| O | 0.122624 | 0.708282 | 0.754443 |
| O | 0.996945 | 0.871776 | 0.118955 |
| O | 0.132779 | 0.495236 | 0.393330 |
| O | 0.377488 | 0.775576 | 0.431223 |
| O | 0.125108 | 0.697988 | 0.076573 |
| O | 0.994003 | 0.871204 | 0.614921 |
| O | 0.789414 | 0.880222 | 0.756807 |
| O | 0.881070 | 0.695238 | 0.574384 |
| O | 0.783648 | 0.884169 | 0.078141 |
| O | 0.873870 | 0.498853 | 0.888080 |
| O | 0.887838 | 0.712571 | 0.929913 |
| O | 0.882616 | 0.702693 | 0.249468 |
| O | 0.699092 | 0.628154 | 0.428444 |
| O | 0.616641 | 0.809525 | 0.576519 |
| O | 0.609691 | 0.796378 | 0.934815 |
| O | 0.614809 | 0.798212 | 0.255061 |
| O | 0.70872 | 0.627346 | 0.751356 |
| O | 0.500011 | 0.632671 | 0.107531 |
| O | 0.874485 | 0.500879 | 0.396796 |
| O | 0.800853 | 0.874278 | 0.433459 |
| O | 0.713772 | 0.62252 | 0.069786 |
| O | 0.506641 | 0.627302 | 0.610750 |

| Atom | X/Y/Z coordinate(Angstrom) |  |  |
| --- | --- | --- | --- |
| Si | 0.168804 | 0.354232 | 0.400805 |
| Si | 0.198909 | 0.391799 | 0.892807 |
| Si | 0.367883 | 0.316376 | 0.596440 |
| Si | 0.136707 | 0.155296 | 0.587061 |
| Si | 0.296171 | 0.102811 | 0.891660 |
| Si | 0.110902 | 0.209065 | 0.079359 |
| Si | 0.345523 | 0.100841 | 0.422543 |
| Si | 0.800531 | 0.399202 | 0.410960 |
| Si | 0.846277 | 0.373787 | 0.894156 |
| Si | 0.898165 | 0.210338 | 0.581911 |
| Si | 0.614060 | 0.302084 | 0.588860 |
| Si | 0.872672 | 0.173872 | 0.085685 |
| Si | 0.668162 | 0.148634 | 0.900712 |
| Si | 0.648236 | 0.360805 | 0.092980 |
| Si | 0.713518 | 0.120801 | 0.396468 |
| Si | 0.285073 | 0.871413 | 0.421301 |
| Si | 0.324258 | 0.857640 | 0.910126 |
| Si | 0.385946 | 0.692387 | 0.600138 |
| Si | 0.101113 | 0.787300 | 0.600924 |
| Si | 0.354791 | 0.655941 | 0.096933 |
| Si | 0.155545 | 0.629796 | 0.904196 |
| Si | 0.124965 | 0.830411 | 0.108721 |
| Si | 0.206684 | 0.598706 | 0.413576 |
| Si | 0.659874 | 0.883362 | 0.420074 |
| Si | 0.702277 | 0.902445 | 0.910995 |
| Si | 0.862947 | 0.841272 | 0.601390 |
| Si | 0.632491 | 0.679199 | 0.599065 |
| Si | 0.884654 | 0.795447 | 0.099429 |
| Si | 0.797643 | 0.614748 | 0.898155 |
| Si | 0.832930 | 0.640583 | 0.406633 |
| Ti | 0.597133 | 0.715242 | 0.098031 |
| Ce | 0.406278 | 0.288006 | 0.130182 |
| O | 0.286611 | 0.374680 | 0.735750 |
| O | 0.383864 | 0.179790 | 0.579881 |
| O | 0.273429 | 0.399665 | 0.057600 |
| O | 0.365820 | 0.983149 | 0.890525 |
| O | 0.385863 | 0.200237 | 0.898318 |
| O | 0.408674 | 0.138930 | 0.260611 |
| O | 0.206584 | 0.109085 | 0.423025 |
| O | 0.126063 | 0.292230 | 0.565491 |
| O | 0.111764 | 0.289943 | 0.918172 |
| O | 0.119993 | 0.289482 | 0.242747 |
| O | 0.202111 | 0.107627 | 0.745641 |
| O | 0.002846 | 0.129648 | 0.091662 |
| O | 0.373340 | 0.969286 | 0.442879 |
| O | 0.309647 | 0.345388 | 0.411688 |
| O | 0.220877 | 0.124235 | 0.063254 |
| O | 0.006270 | 0.124150 | 0.588728 |
| O | 0.890195 | 0.296681 | 0.739104 |
| O | 0.795319 | 0.125510 | 0.558057 |
| O | 0.888456 | 0.309489 | 0.061185 |
| O | 0.629448 | 0.020632 | 0.905316 |
| O | 0.805202 | 0.135023 | 0.919840 |
| O | 0.796873 | 0.128301 | 0.236517 |
| O | 0.623621 | 0.227646 | 0.415693 |
| O | 0.711466 | 0.394024 | 0.568688 |
| O | 0.709319 | 0.387906 | 0.918333 |
| O | 0.727331 | 0.391987 | 0.245620 |
| O | 0.626358 | 0.215066 | 0.739560 |
| O | 0.525526 | 0.413464 | 0.124735 |
| O | 0.631257 | 0.016134 | 0.403922 |
| O | 0.891950 | 0.294047 | 0.423749 |
| O | 0.620545 | 0.224138 | 0.062983 |
| O | 0.491902 | 0.367012 | 0.602458 |
| O | 0.369487 | 0.780713 | 0.754159 |
| O | 0.290751 | 0.598183 | 0.575026 |
| O | 0.369376 | 0.793405 | 0.076385 |
| O | 0.117514 | 0.503314 | 0.870325 |
| O | 0.292313 | 0.617358 | 0.926654 |
| O | 0.283502 | 0.608344 | 0.249155 |
| O | 0.112282 | 0.701048 | 0.438971 |
| O | 0.203110 | 0.872651 | 0.584314 |
| O | 0.187868 | 0.874459 | 0.943091 |
| O | 0.199083 | 0.872273 | 0.265024 |
| O | 0.109714 | 0.706715 | 0.756888 |
| O | 0.993888 | 0.872092 | 0.122494 |
| O | 0.135872 | 0.485820 | 0.405110 |
| O | 0.372624 | 0.763257 | 0.430272 |
| O | 0.113686 | 0.694108 | 0.077220 |
| O | 0.992649 | 0.873615 | 0.609355 |
| O | 0.792628 | 0.892406 | 0.758845 |
| O | 0.875460 | 0.704422 | 0.574633 |
| O | 0.779295 | 0.886690 | 0.078419 |
| O | 0.879791 | 0.502808 | 0.876425 |
| O | 0.884133 | 0.716442 | 0.929558 |
| O | 0.876692 | 0.707748 | 0.249653 |
| O | 0.695157 | 0.638134 | 0.424340 |
| O | 0.617183 | 0.816949 | 0.584007 |
| O | 0.609656 | 0.805156 | 0.917107 |
| O | 0.604516 | 0.817714 | 0.266900 |
| O | 0.709706 | 0.630303 | 0.746636 |
| O | 0.484723 | 0.616572 | 0.105536 |
| O | 0.874391 | 0.510161 | 0.408810 |
| O | 0.797888 | 0.883490 | 0.435687 |
| O | 0.716975 | 0.615362 | 0.063472 |
| O | 0.508468 | 0.629834 | 0.611473 |

* Corresponding author. Tel: +86-912-3891144; Fax: +86-912-3891144

E-mail address: liguogao2008@163.com