Supplementary: Mechano-chemically activated fly-ash and sisal fiber reinforced PP hybrid composite with enhanced mechanical properties

Atul Kumar Maurya1, Rupam Gogoi1, Gaurav Manik1*

1Department of Polymer and Process Engineering, Indian Institute of Technology Roorkee, Saharanpur Campus, Paper Mill Road, Saharanpur-247001, UP, India.

#First author, e-mail id: amaurya@pe.iitr.ac.in

*Corresponding author, e-mail id: manikfpt@iitr.ac.in, gaurav.manik@pe.iitr.ac.in, gauravmanik3m@gmail.com; Contact: +91 1322714340

Fig.S1. DLS image for the most probable size of the fly ash particle after high energy ball milling.

Density measurement

Density of all the composites have been calculated using the Equation S1, Table S1 depicts the value of all the samples.

Density gmcm3   =Wair   gmVf-Vi cm3            S1

Where, Wair - weight of the sample in the air, Vf = Final volume of the liquid media (water) and Vi= Initial volume of the liquid media.

| Table S1: Density calculation of polymer, blends and composite |  |  |  |
| --- | --- | --- | --- |
| Sample | Weight (gm) | Vf - Vi (cm3) | ~Density (gm/cm3) Calculated |
| PP | 1.238 | 1.4 | 0.88 |
| BM | 1.014 | 1.10 | 0.92 |
| SSL | NA | NA | 1.45 |
| FA | NA | NA | 0.83 |
| C | 1.01 | 0.9 | 0.89 |
| H1 | 1.207 | 1.10 | 1.10 |
| H2 | 1.339 | 1.30 | 1.03 |
| H3 | 1.05 | 1.02 | 1.03 |