Supplementary Information

Regulation mechanism of graphene oxide on the structure and mechanical properties of bio-based gel-spun lignin/poly (vinyl alcohol) fibers

Yanhong Jin1,2, Yuanyuan Jing1,2, Wenxin Hu1,2, Jiaxian Lin1,2, Yu Cheng1,2, Xiaona Yang1,2, Kun Zhang1,2, Chunhong Lu1,2*

1 Key Laboratory of Textile Science & Technology, Ministry of Education, Donghua University, Shanghai 201620, China

2 College of Textiles, Donghua University, Shanghai 201620, China

* Corresponding author’s e-mail address: chlu@dhu.edu.cn

Calibration curve for the estimation of fiber percent crystallinity from FTIR spectra

The X-ray diffraction (XRD) of 0.05% GO/5% lignin/PVA fiber, 0.2% GO/5% lignin/PVA fiber, and 0.2% GO/PVA fiber, was performed on the Rigaku D/max-2550 PC X-ray Diffractometer with Cu Kα radiation (λ = 1.541 Å), operating voltage of 40 kV and current of 150 mA. Shredded fiber powders were scanned at 0.06 °/s in the 2θ range of 5-55° (Fig. S1). Peak fitting was performed by MDI Jade 6 software. The percent crystallinity (Xc) of each fiber was calculated from crystalline (Ac) and amorphous (Aa) peak areas with the following equation(Minus et al. 2006):

Xc%=AcAc+Aa×100%                                                (1)

The percent crystallinity of polymer is estimated by the following equation (Peppas 1977; Tretinnikov and Zagorskaya 2012):

Xc=a+bA1114A854×100%                                                 (2)

where a and b are constants whose values are calculated from known values of percent crystallinity from X-ray diffraction, A1144 and A854 are infrared spectra absorbance at 1144 cm-1 and 854 cm-1, respectively.

With known values of percent crystallinity (Xc) obtained from XRD data (Fig. S1) and values of A1144/A854 obtained from infrared spectra (Table S1), the exact values of a and b were determined by linear regression using OriginPro 9 software.

Fig. S1 XRD diffractograms of composite fibers

Table S1. Fiber percent crystallinity from XRD and A1144/A854 infrared absorbance ratio

| Sample | Percent crystallinity(Xc)/% | A1144/A854 |
| --- | --- | --- |
| 0.05% GO/5% lignin/PVA fiber | 59.70 | 2.44 |
| 0.2% GO/5% lignin/PVA fiber | 56.40 | 2.29 |
| 0.2%GO/PVA fiber | 51.78 | 1.91 |

Data in Table S1 yielded a calibration curve shown in Figure S2. The intercept and slope of the fitted curve were constants a=14.40 and b=24.09, respectively.

Fig. S2 Linear regression curve indicating the relationship between percent crystallinity (Xc) by XRD and A1144/A854 IR absorbance ratio from lignin/PVA, GO/PVA and lignin/GO/PVA fibers

Imaging analysis by SEM

Fig. S3 (a) Low- and (b) high-resolution SEM images of fracture tips of 0.2% GO/PVA fibers after mechanical testing

Fiber orientation analysis by XRD patterns

Fig. S4 XRD diffractograms of aligned composite fiber bundles

Moisture resistance of fiber

Fig. S5 Optical micrographs of 0.2% GO/PVA fiber after water immersion at (a) 25 and (b) 85 °C

References:

Minus ML, Chae HG, Kumar S (2006) Single wall carbon nanotube templated oriented crystallization of poly(vinyl alcohol). Polymer 47:3705-3710 doi:10.1016/j.polymer.2006.03.076

Peppas NA (1977) Infrared spectroscopy of semicrystalline poly(vinyl alcohol) networks. Macromolecular Chemistry and Physics 178:596-601

Tretinnikov ON, Zagorskaya SA (2012) Determination of the degree of crystallinity of poly(vinyl alcohol) by FTIR spectroscopy. Journal of Applied Spectroscopy 79:521-526