Supporting Information for

An Environmentally Friendly Phosphorus-Modified Cellulose/Silica Hybrid Hydrogel for Fire Prevention and Firefighting

Hafezeh Nabipour a, Hu Shi a, Xin Wang a,*, Xiangming Hu b, Lei Song a, Yuan Hu a,*

a State Key Laboratory of Fire Science, University of Science and Technology of China, 96 Jinzhai Road, Hefei, Anhui 230026, P. R. China.

b Key Lab of Mine Disaster Prevention and Control, College of Mining ad Safety Engineering, Shandong University of Science and Technology, Qingdao, Shandong 266590, P. R. China.

*Corresponding authors. Tel/Fax: +86-551-63601664. E-mail address: yuanhu@ustc.edu.cn (Y. Hu), wxcmx@ustc.edu.cn (X. Wang).

Table S1. Power law and Herschel-Bulkley parameters for steady flow measurement.

| Sample | Power law parameter |  |  | Herschel-Bulkley parameter |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | k | n | R2 | τ0 | k | n | R2 |
| H1 | 6.0735 | 0.6650 | 0.9937 | 1.5564 | 6.8003 | 0.6401 | 0.9998 |
| H2 | 11.663 | 0.6803 | 0.9991 | 1.4835 | 13.1990 | 0.6530 | 0.9996 |
| H3 | 1.1446 | 0.6704 | 0.9997 | 0.1744 | 3.3436 | 0.6755 | 0.9998 |
| H4 | 16.386 | 0.4640 | 0.9975 | 5.4227 | 12.595 | 0.5201 | 0.9995 |
| H5 | 85.465 | 0.2312 | 0.9836 | 48.9581 | 38.603 | 0.3763 | 0.9987 |

Table S2. Power law parameters for storage (G') and loss (G") moduli.

| Sample | G’ |  |  | G” |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | a1 | b1 | R2 | a2 | b2 | R2 |
| H1 | 1.1896 | 0.8646 | 0.9990 | 4.5226 | 0.6427 | 0.9965 |
| H2 | 2.1970 | 0.9328 | 0.9967 | 13.442 | 0.5738 | 0.9920 |
| H3 | 0.4147 | 0.9991 | 0.9948 | 2.8689 | 0.6784 | 0.9946 |
| H4 | 9.3471 | 0.5681 | 0.9989 | 10.111 | 0.5501 | 0.9986 |
| H5 | 173.73 | 0.2243 | 0.9953 | 31.680 | 0.4274 | 0.9987 |

Fig. S1. The applied fire-extinguishing test set-up.

Fig. S2. The temperature versus time plots of firefighting experiments using (a) water, (b) H1, (c) H2, and (d) H4.

#### Fig. S3. XRD pattern of the char residue of wood quenched by H4 hydrogel.