Supplementary Information

Fluorine anion modification of high-voltage Mn-rich phosphate cathodes for high-power and long-lasting sodium-ion batteries

Wei Zhang, 1, 2, 5 Yulun Wu, 1,5 Zhenming Xu, 3, * Jianwei Li, 2 Yuhang Dai, 2 Wei Zong, 2 Ruwei Chen, 2 Shihao Li, 1 Fei Guo, 2 Simin Li, 1Feixiang Wu, 1 Zhian Zhang,1,* Guanjie He,2 ,4* Yanqing Lai,1,* and Ivan P. Parkin,2,*

1 School of Metallurgy and Environment, Engineering Research Center of the Ministry of Education for Advanced Battery Materials, Hunan Provincial Key Laboratory of Nonferrous Value-Added Metallurgy, Central South University, Changsha 410083, P. R. China

2 Christopher Ingold Laboratory, Department of Chemistry, University College London, London WC1H 0AJ, UK

3 Jiangsu Key Laboratory of Electrochemical Energy Storage Technologies, College of Materials Science and Technology, Nanjing University of Aeronautics and Astronautics, Nanjing 210016, P. R. China

4 Electrochemical Innovation Lab (EIL), Department of Chemical Engineering, University College London, London WC1E 7JE, UK

5 These authors contributed equally: Wei Zhang, Yulun Wu.

*E-mail: xuzhenming@nuaa.edu.cn; zhangzhian@csu.edu.cn; g.he@ucl.ac.uk; laiyanqing@csu.edu.cn; i.p.parkin@ucl.ac.uk

Supplementary Figures and Tables

Supplementary Fig. 1 Comparison of X-ray diffraction (XRD) results of different as-prepared samples.

Supplementary Fig. 2 XRD Rietveld refinement results of Na4-3xMnCr(PO4-xFx)3.

Supplementary Table 1 Detailed structural information of NMCP (0F) derived from Rietveld refinement.

| Space group = R_3c |  | Rwp = 1.48% |  | Rp = 1.16% |  |
| --- | --- | --- | --- | --- | --- |
| a (Å) = 8.915 |  | c (Å) = 21.422 |  | α (°) = 90 |  |
| β (°) = 90 |  | γ (°) = 120 |  | V (Å3) = 1474.323 |  |
| Atom | x | y | z | frac | site |
| Na1 | 0.00000 | 0.00000 | 0.00000 | 1.040 | 6b |
| Na2 | 0.64984 | 0.00000 | 0.25000 | 0.971 | 18e |
| Mn | 0.00000 | 0.00000 | 0.14935 | 0.500 | 12c |
| Cr | 0.00000 | 0.00000 | 0.14935 | 0.500 | 12c |
| P | 0.29936 | 0.00000 | 0.25000 | 1.000 | 18e |
| O1 | 0.01594 | 0.21084 | 0.19159 | 1.000 | 36f |
| O2 | 0.18785 | 0.17284 | 0.08423 | 1.000 | 36f |

Supplementary Table 2 Detailed structural information of 0.01F derived from Rietveld refinement.

| Space group = R_3c |  | Rwp = 1.32% |  | Rp = 1.04% |  |
| --- | --- | --- | --- | --- | --- |
| a (Å) = 8.919 |  | c (Å) = 21.443 |  | α (°) = 90 |  |
| β (°) = 90 |  | γ (°) = 120 |  | V (Å3) = 1477.099 |  |
| Atom | x | y | z | frac | site |
| Na1 | 0.00000 | 0.00000 | 0.00000 | 1.003 | 6b |
| Na2 | 0.64209 | 0.00000 | 0.25000 | 0.943 | 18e |
| Mn | 0.00000 | 0.00000 | 0.15135 | 0.500 | 12c |
| Cr | 0.00000 | 0.00000 | 0.15135 | 0.500 | 12c |
| P | 0.29683 | 0.00000 | 0.25000 | 1.000 | 18e |
| O1 | 0.01650 | 0.21000 | 0.19300 | 0.998 | 36f |
| O2 | 0.18569 | 0.17236 | 0.08364 | 0.998 | 36f |
| F1 | 0.01650 | 0.21000 | 0.19300 | 0.002 | 36f |
| F2 | 0.18569 | 0.17236 | 0.08364 | 0.002 | 36f |

Supplementary Table 3 Detailed structural information of 0.02F derived from Rietveld refinement.

| Space group = R_3c |  | Rwp = 1.31% |  | Rp = 1.04% |  |
| --- | --- | --- | --- | --- | --- |
| a (Å) = 8.916 |  | c (Å) = 21.414 |  | α (°) = 90 |  |
| β (°) = 90 |  | γ (°) = 120 |  | V (Å3) = 1474.182 |  |
| Atom | x | y | z | frac | site |
| Na1 | 0.00000 | 0.00000 | 0.00000 | 1.266 | 6b |
| Na2 | 0.63993 | 0.00000 | 0.25000 | 1.055 | 18e |
| Mn | 0.00000 | 0.00000 | 0.15015 | 0.500 | 12c |
| Cr | 0.00000 | 0.00000 | 0.15015 | 0.500 | 12c |
| P | 0.29976 | 0.00000 | 0.25000 | 1.000 | 18e |
| O1 | 0.01696 | 0.20785 | 0.19541 | 0.995 | 36f |
| O2 | 0.18717 | 0.17457 | 0.08400 | 0.995 | 36f |
| F1 | 0.01696 | 0.20785 | 0.19541 | 0.005 | 36f |
| F2 | 0.18717 | 0.17457 | 0.08400 | 0.005 | 36f |

Supplementary Table 4 Detailed structural information of NMCPF (0.05F) derived from Rietveld refinement.

| Space group = R_3c |  | Rwp = 1.52% |  | Rp = 1.18% |  |
| --- | --- | --- | --- | --- | --- |
| a (Å) = 8.907 |  | c (Å) = 21.409 |  | α (°) = 90 |  |
| β (°) = 90 |  | γ (°) = 120 |  | V (Å3) = 1470.906 |  |
| Atom | x | y | z | frac | site |
| Na1 | 0.00000 | 0.00000 | 0.00000 | 1.058 | 6b |
| Na2 | 0.63891 | 0.00000 | 0.25000 | 0.948 | 18e |
| Mn | 0.00000 | 0.00000 | 0.14920 | 0.500 | 12c |
| Cr | 0.00000 | 0.00000 | 0.14920 | 0.500 | 12c |
| P | 0.29689 | 0.00000 | 0.25000 | 1.000 | 18e |
| O1 | 0.02285 | 0.20794 | 0.19536 | 0.988 | 36f |
| O2 | 0.18276 | 0.17623 | 0.08464 | 0.988 | 36f |
| F1 | 0.02285 | 0.20794 | 0.19536 | 0.012 | 36f |
| F2 | 0.18276 | 0.17623 | 0.08464 | 0.012 | 36f |

Supplementary Table 5 Detailed structural information of 0.1F derived from Rietveld refinement.

| Space group = R_3c |  | Rwp = 2.30% |  | Rp = 1.60% |  |
| --- | --- | --- | --- | --- | --- |
| a (Å) = 8.921 |  | c (Å) = 21.398 |  | α (°) = 90 |  |
| β (°) = 90 |  | γ (°) = 120 |  | V (Å3) = 1474.886 |  |
| Atom | x | y | z | frac | site |
| Na1 | 0.00000 | 0.00000 | 0.00000 | 1.168 | 6b |
| Na2 | 0.64161 | 0.00000 | 0.25000 | 1.052 | 18e |
| Mn | 0.00000 | 0.00000 | 0.16000 | 0.500 | 12c |
| Cr | 0.00000 | 0.00000 | 0.16000 | 0.500 | 12c |
| P | 0.30093 | 0.00000 | 0.25000 | 1.000 | 18e |
| O1 | 0.02760 | 0.21321 | 0.19434 | 0.975 | 36f |
| O2 | 0.19387 | 0.17092 | 0.08709 | 0.975 | 36f |
| F1 | 0.02760 | 0.21321 | 0.19434 | 0.025 | 36f |
| F2 | 0.19387 | 0.17092 | 0.08709 | 0.025 | 36f |

Supplementary Table 6 Detailed structural information of 0.15F derived from Rietveld refinement.

| Space group = R_3c |  | Rwp = 3.40% |  | Rp = 2.17% |  |
| --- | --- | --- | --- | --- | --- |
| a (Å) = 8.931 |  | c (Å) = 21.380 |  | α (°) = 90 |  |
| β (°) = 90 |  | γ (°) = 120 |  | V (Å3) = 1476.950 |  |
| Atom | x | y | z | frac | site |
| Na1 | 0.00000 | 0.00000 | 0.00000 | 0.941 | 6b |
| Na2 | 0.64377 | 0.00000 | 0.25000 | 0.989 | 18e |
| Mn | 0.00000 | 0.00000 | 0.14700 | 0.500 | 12c |
| Cr | 0.00000 | 0.00000 | 0.14700 | 0.500 | 12c |
| P | 0.30176 | 0.00000 | 0.25000 | 1.000 | 18e |
| O1 | 0.02658 | 0.20495 | 0.19196 | 0.962 | 36f |
| O2 | 0.20857 | 0.17458 | 0.09034 | 0.962 | 36f |
| F1 | 0.02658 | 0.20495 | 0.19196 | 0.038 | 36f |
| F2 | 0.20857 | 0.17458 | 0.09034 | 0.038 | 36f |

Supplementary Fig. 3 Rate performances of Na4-3xMnCr(PO4-xFx)3 samples under 1.5-4.3 V (vs. Na+/Na).

Supplementary Fig. 4 Bond length of Na(2)-O for Na4-3xMnCr(PO4-xFx)3 samples.

Supplementary Fig. 5 ICP results of a NMCPF and b NMCP.

Supplementary Fig. 6 a TEM and b HRTEM images (inset: FFT pattern), c SAED pattern and d EDS mapping images of NMCP sample.

Supplementary Fig. 7 Solid-state 19F NMR spectra of the pristine NMCPF and the reference NaF. The asterisks indicate spinning sidebands (SSBs).

Supplementary Fig. 8 TG results of a NMCPF and b NMCP.

Supplementary Fig. 9 FT-IR results of a NMCPF and b NMCP.

Supplementary Fig. 10 Raman spectra of NMCPF and NMCP.

Supplementary Fig. 11 XPS spectra of NMCPF and NMCP.

Supplementary Fig. 12 Cycling stability at 0.1 C for NMCPF and NMCP within 1.5–4.3 V.

Supplementary Fig. 13 Cycling stability at 0.5 C for NMCPF and NMCP within 1.5–4.3 V.

Supplementary Fig. 14 Cycling stability at 5 C for NMCPF and NMCP within 1.5–4.3 V.

Supplementary Fig. 15 Cycling stability at 10 C for NMCPF and NMCP within 1.5–4.3 V.

Supplementary Fig. 16 Electrochemical capabilities within 1.5–4.5 V. a CV curves at 0.1 mV s-1. b Initial charge/discharge curve at 0.1 C. c Rate properties. d Cycling capabilities at 1 C.

Supplementary Fig. 17 Kinetics properties of NMCPF and NMCP. a GITT profiles and corresponding b DNa+ as well as c overpotentials. d DNa+ obtained from CV methods at various scan rates.

Supplementary Fig. 18 Detailed schematic diagram of a single-step GITT experiment at ~3.6 V for NMCPF cathode (current density: 0.1 C, 11 mA g-1).

GITT calculation. 1200 s (τ) was set as the charging time, followed by a rest time of 3600 s. To calculate the diffusion coefficient of Na+ (D), the equation is as follow1:

D = 4 πτmBVmMBS2∆Es∆Eτ2           τ≪L2/D     (Supplementary Equation 1)

Where L, mB, MB, Vm, S represent the thickness of the electrode, mass, molecular weight, molar volume, surface area of NMCPF or NMCP.

Supplementary Fig. 19 a CV curves at various scan rates from 0.1 to 1.0 mV s-1 and b the linear fitting for the relationship between ip and v1/2 from CV profiles of NMCPF. c CV curves at various scan rates from 0.1 to 1.0 mV s-1 and d the linear fitting for the relationship between ip and v1/2 from CV profiles of NMCP.

The DNa+ from CV tests can be calculated based on the Randles-Sevcik equation2, 3:

ip = 2.69 × 105n3/2AD1/2Cv1/2  (Supplementary Equation 2)

Where ip refers to the peak current, n (2 in this test) is the amounts of transferred electrons, A (0.785 cm2) is the surface area of electrode, C represents the Na+ molar concentration (2.66 × 10-2 mol cm-3), and v refers to the scan rates.

Supplementary Fig. 20 Full scope of in-situ XRD patterns of a NMCPF and b NMCP.

Supplementary Fig. 21 Ex-situ XPS spectra of Mn 2p3/2 and Cr 2p3/2 of a NMCPF and b NMCP at different charging states.

Supplementary Table 7 Magnetic moments of Mn, Cr, and F sites in NaxMnCr(PO3.95F0.05)3 (x= 3.85, 2.85, 1.85 and 0.85).

| Compositions | Magnetic Moment (μB) |  |  |
| --- | --- | --- | --- |
|  | Mn×6 | Cr×6 | F×1 |
| Na3.85MnCr(PO3.95F0.05)3 | 4.462 4.46 4.464 4.463 4.471 4.451 | 2.817 2.829 2.835 2.841 2.83 2.829 | 0.012 |
| Na2.85MnCr(PO3.95F0.05)3 | 3.595 3.593 3.465 3.766 3.635 3.561 | 2.588 2.739 2.679 2.685 2.722 2.722 | 0.013 |
| Na1.85MnCr(PO3.95F0.05)3 | -3.357 -3.329 -3.419 -3.351 -3.398 -3.685 | -2.548 2.592 2.6 -2.617 2.62 2.622 | -0.018 |
| Na0.85MnCr(PO3.95F0.05)3 | 2.699 2.679 2.715 2.719 2.735 2.702 | 1.966 2.069 1.884 2.037 2.005 1.95 | 0.002 |

Supplementary Table 8 Magnetic moments of Mn and Cr sites in NaxMnCr(PO4)3 (x= 4, 3, 2 and 1).

| Compositions | Magnetic Moment (μB) |  |
| --- | --- | --- |
|  | Mn×6 | Cr×6 |
| Na4MnCr(PO4)3 | 4.63×6 | 2.93×6 |
| Na3MnCr(PO4)3 | 3.868×6 | 2.912×6 |
| Na2MnCr(PO4)3 | 3.23×6 | 2.886×6 |
| Na1MnCr(PO4)3 | 3.115×6 | -2.56×6 |

Supplementary Fig. 22 DOS patterns of a NMCPF and b NMCP with different Na contents.

Supplementary Table 9 Integrated crystal orbital Hamilton population (ICOHP) of Mn-O or Mn-F bonds in NMCPF.

| Type of bond | Distance / Å | Spin direction | ICOHP / eV |
| --- | --- | --- | --- |
| Mn29-F125 | 2.49 | Spin up | -0.09 |
|  |  | Spin down | -0.16 |
| Mn29-O121 | 2.24 | Spin up | -0.18 |
|  |  | Spin down | -0.32 |
| Mn29-O120 | 2.20 | Spin up | -0.25 |
|  |  | Spin down | -0.43 |
| Mn29-O86 | 2.06 | Spin up | -0.60 |
|  |  | Spin down | -0.86 |
| Mn29-O85 | 2.13 | Spin up | -0.41 |
|  |  | Spin down | -0.58 |
| Mn29-O84 | 2.07 | Spin up | -0.36 |
|  |  | Spin down | -0.66 |
| Accumulated ICOHP / eV |  |  | -4.91 |

Supplementary Table 10 Integrated crystal orbital Hamilton population (ICOHP) of Mn-O bonds in NMCP.

| Type of bond | Distance / Å | Spin direction | ICOHP / eV |
| --- | --- | --- | --- |
| Mn30-O123 | 2.25 | Spin up | -0.15 |
|  |  | Spin down | -0.31 |
| Mn30-O122 | 2.25 | Spin up | -0.15 |
|  |  | Spin down | -0.31 |
| Mn30-O121 | 2.25 | Spin up | -0.15 |
|  |  | Spin down | -0.31 |
| Mn30-O87 | 2.12 | Spin up | -0.41 |
|  |  | Spin down | -0.59 |
| Mn30-O86 | 2.12 | Spin up | -0.41 |
|  |  | Spin down | -0.59 |
| Mn30-O85 | 2.12 | Spin up | -0.41 |
|  |  | Spin down | -0.59 |
| Accumulated ICOHP / eV |  |  | -4.38 |

Supplementary Fig. 23 COHP and ICOHP results of Mn29 atom interacting with different O/F atoms around it in NMCPF.

Supplementary Fig. 24 COHP and ICOHP results of Mn30 atom interacting with different O atoms around it in NMCP.

Supplementary References

1.	Rui X. H., Ding N., Liu J., Li C. & Chen C. H. Analysis of the chemical diffusion coefficient of lithium ions in Li3V2(PO4)3 cathode material. Electrochim. Acta 55, 2384-2390 (2010).

2.	Gu Z. Y. et al. An Advanced High-Entropy Fluorophosphate Cathode for Sodium-Ion Batteries with Increased Working Voltage and Energy Density. Adv. Mater. 34, 2110108 (2022).

3.	Zhang J. et al. A Novel NASICON‐Type Na4MnCr(PO4)3 Demonstrating the Energy Density Record of Phosphate Cathodes for Sodium‐Ion Batteries. Adv. Mater. 32, 1906348 (2020).