Supporting Information for

Influence of the Metal−Support and Metal−Metal Interactions on

Pd nucleation and NO adsorption in a Pd4/γ-Al2O3 (110D) model

Letícia M. Prates,a José W. de M. Carneirob and Maurício T. de M. Cruz a*

aDepartamento de Química Geral e Inorgânica. Instituto de Química. Universidade do Estado do Rio de Janeiro. Campus Maracanã. 20550-900. Rio de Janeiro-RJ. Brasil.

bDepartamento de Química Inorgânica. Instituto de Química. Universidade Federal Fluminense. Campus do Valonguinho. 24020-141. Niterói-RJ. Brasil.

*Corresponding author: mauricio.cruz@uerj.br

Contents:

Fig. S1 Approximation modes of the planar Pd4 cluster on the (110D) face of the Al13O23H7 model and its respective resulting structures from the optimization process, with absolute energies (in Hartree) in 6-31G(d) and LANL2DZ (between parenthesis): (a, a’, a’’) parallel and (b, b’, b’’) perpendicular……………………………………...……..S3

Fig. S2 Pd−ion distances at (110D) surface of the Al13O23H7 model..……………………………………….…...….S4

Fig. S3 LMOEDA (energy in kcal mol-1) in the Pd1(sp)/Al13O23H7 complex…………………………….…………...S4

Fig. S4 Front view of resulting NO/Pd4(boat) agglomerates………………………………………….…….………….S5

Fig. S5 Ion numbering in the Al13O23H7 γ-alumina model..………………………........................................……….S5

Fig. S6 Front view of resulting NO/Pd4 agglomerates in planar and tetrahedral arrangements…...………………..S18

Table S1 Experimental geometric parameters for bulk γ-alumina (bond distances (d) and bond angles (a))........….S5

Table S2 Relative energy (Erel) and spin contamination (S2 and S2(A), A=annihilated) calculated for Al13O23H7, Pd4/Al13O23H7 and Pd5/Al13O23H7 aggregates in different electronic spin states (ESS) with B3LYP functional and the 6-31G(d) and LANL2DZ/6-31G(d) basis sets, respectively………………………………………………………....S6

Table S3 Charge distribution (q) on γ-alumina ions and Pd atoms in Al13O23H7, Pd4/Al13O23H7, and Pd5/Al13O23H7 aggregates, calculated with NBO, Hirshfeld (Hirsh.), Merz-Singh-Kollman (MSK), and Mulliken (Mul.) methods.........................................................................................................................................................................S7

Table S4 Bond distance (d) and bond angle (a) in Pd4 clusters with planar (in D2h symmetry, single point) and tetrahedral (in Cs, resulting from the optimization of the isolated planar form, and Td, single point, symmetries) arrangements.................................................................................................................................................................S9

Table S5 Bonding energy of each palladium atom in: Pd4/Al13O23H7 complex (Eb(Pd4/sup)) and boat Pd4 (Eb(Pd4)) and    γ-alumina (Eb(sup)) moieties...........................................................................................................................................S9

Table S6 Charge distribution (q) in the Pd1(sp)/Al13O23H7 complexes calculated with NBO, Hirshfeld, Merz-Singh-Kollman, and Mulliken methods................................................................................................................................S10

Table S7 Bond distances (d) in Pd5/Al13O23H7 complex............................................................................................S12

Table S8 Charge distribution (q) on the palladium atoms in the isolated Pd4 and Pd5 clusters (obtained in the presence of γ-alumina) calculated with the NBO, Hirshfeld (Hirsh.), Merz-Singh-Kollman (MSK), and Mulliken (Mul.) methods............................................................................................................................................................S12

Table S9 Relative energy (Erel) and spin contamination (S2 and S2(A), A=annihilated) calculated for the NO/Pd4/Al13O23H7 and NO/Pd4(boat) clusters in different electronic spin states (ESS) with the B3LYP functional and the 6-311+G(d)/LANL2DZ/6-31G(d) and 6-311+G(d)/LANL2DZ basis sets, respectively.....................................S13

Table S10 Charge distribution (q) in the NO/Pd4/Al13O23H7 complexes calculated with NBO, Hirshfeld, Merz-Singh-Kollman, and Mulliken methods......................................................................................................................S14

Table S11 Adsorption energy (Ead) for NO molecule on isolated boat Pd4 clusters, in bridge and hollow modes, geometric parameters (bond distance (d) and bond angle (a)) and NBO charge (q) on γ-alumina, Pd4, Pd atom bonded to NO and NO moieties..................................................................................................................................S16

Table S12 Charge distribution (q) in the NO/Pd4(boat) agglomerates, calculated with NBO, Hirshfeld, Merz-Singh-Kollman, and Mulliken methods................................................................................................................................S17

Table S13 Adsorption energy (Ead, in kcal mol-1) for NO molecule on isolated Pd4 clusters, in planar and tetrahedral arrangements, geometric parameters (bond distance, in Å, and bond angle, in °) and NBO charge (in ē) on γ-alumina, Pd4, Pd atom bonded to NO and NO moieties…………………………………………………..…...S19

Fig. S1 Approximation modes of the planar Pd4 cluster on the (110D) face of the Al13O23H7 model and its respective resulting structures from the optimization process, with absolute energies (in Hartree) in 6-31G(d) and LANL2DZ (between parenthesis): (a, a’, a’’) parallel and (b, b’, b’’) perpendicular

Fig. S2 Pd−ion distances at (110D) surface of the Al13O23H7 model

Fig. S3  LMOEDA (energy in kcal mol-1) in the Pd1(sp)/Al13O23H7 complex

Fig. S4 Front view of resulting NO/Pd4(boat) agglomerates

Fig. S5 Ion numbering in the Al13O23H7 γ-alumina model

Table S1 Experimental geometric parameters for bulk γ-alumina (bond distances (d) and bond angles (a))

| dAlo–O (Å) | 1.97 |
| --- | --- |
| dAlt–O (Å) | 1.71 |
| aO–Alo–O (°) | 90.00/180.00 |
| aO–Alt–O (°) | 109.47 |
| aAlo–O–Alo (°) | 90.00 |
| aAlt–O–Alo (°) | 125.30 |

Table S2 Relative energy (Erel) and spin contamination (S2 and S2(A), A=annihilated) calculated for Al13O23H7, Pd4/Al13O23H7 and Pd5/Al13O23H7 aggregates in different electronic spin states (ESS) with B3LYP functional and the 6-31G(d) and LANL2DZ/6-31G(d) basis sets, respectively

|  |  | Al13O23H7 |  |  |  | Pd4/Al13O23H7 |  |  |  | Pd5/Al13O23H7 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ESS | S | S2 | S2 (A) | Erel (kcal mol-1) |  | S2 | S2(A) | Erel (kcal mol-1) |  | S2 | S2(A) | Erel (kcal mol-1) |
| Singlet | 0 | 0.00 | 0.00 | 0.00 |  | 0.00 | 0.00 | 5.99 |  | 0.00 | 0.00 | 4.98 |
| Triplet | 1 | 2.02 | 2.00 | 2.94 |  | 2.03 | 2.00 | 0.00 |  | 2.03 | 2.00 | 0.00 |
| Quintuplet | 2 | 6.04 | 6.00 | 43.11 |  | 6.07 | 6.00 | 15.84 |  | 6.05 | 6.00 | 15.70 |
| Septet | 3 | 12.04 | 12.00 | 102.11 |  | 12.05 | 12.00 | 38.50 |  | 12.06 | 12.00 | 37.22 |

Table S3 Charge distribution (q) on γ-alumina ions and Pd atoms in Al13O23H7, Pd4/Al13O23H7, and Pd5/Al13O23H7 aggregates, calculated with NBO, Hirshfeld (Hirsh.), Merz-Singh-Kollman (MSK), and Mulliken (Mul.) methods

|  | Al13O23H7 |  |  |  |  | Pd4/Al13O23H7 |  |  |  |  | Pd5/Al13O23H7 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom/q (ē) | NBO | Hirsh. | MSK | Mul. |  | NBO | Hirsh. | MSK | Mul. |  | NBO | Hirsh. | MSK | Mul. |
| Al(1) | +1.950 | +0.653 | +1.760 | +1.079 |  | +1.952 | +0.621 | +1.744 | +1.086 |  | +1.916 | +0.537 | +1.791 | +1.114 |
| Al(2) | +1.877 | +0.577 | +1.558 | +0.905 |  | +1.906 | +0.565 | +1.552 | +0.873 |  | +1.954 | +0.588 | +1.568 | +0.979 |
| Al(3) | +1.877 | +0.577 | +1.558 | +0.905 |  | +1.906 | +0.565 | +1.552 | +0.873 |  | +1.953 | +0.593 | +1.591 | +0.969 |
| Al(4) | +1.988 | +0.658 | +1.616 | +1.019 |  | +2.060 | +0.675 | +1.641 | +1.064 |  | +2.080 | +0.665 | +1.833 | +1.078 |
| Al(5) | +1.913 | +0.630 | +1.605 | +1.110 |  | +1.695 | +0.376 | +1.234 | +1.223 |  | +1.789 | +0.451 | +1.390 | +1.367 |
| Al(6) | +1.913 | +0.630 | +1.605 | +1.110 |  | +1.695 | +0.376 | +1.234 | +1.223 |  | +1.697 | +0.370 | +1.165 | +1.375 |
| Al(7) | +1.830 | +0.509 | +1.129 | +1.110 |  | +1.881 | +0.512 | +1.156 | +1.163 |  | +1.828 | +0.487 | +0.981 | +1.123 |
| Al(8) | +1.830 | +0.509 | +1.129 | +1.110 |  | +1.881 | +0.512 | +1.156 | +1.163 |  | +1.850 | +0.494 | +0.996 | +1.134 |
| Al(9) | +1.720 | +0.645 | +1.370 | +0.937 |  | +1.750 | +0.649 | +1.391 | +0.921 |  | +1.729 | +0.623 | +1.345 | +0.878 |
| Al(10) | +1.720 | +0.645 | +1.370 | +0.937 |  | +1.750 | +0.649 | +1.391 | +0.921 |  | +1.759 | +0.640 | +1.397 | +0.887 |
| Al(11) | +1.950 | +0.683 | +1.567 | +1.028 |  | +1.887 | +0.581 | +1.469 | +0.980 |  | +1.908 | +0.609 | +1.426 | +0.956 |
| Al(12) | +1.994 | +0.678 | +1.527 | +0.992 |  | +2.022 | +0.681 | +1.545 | +0.973 |  | +2.002 | +0.661 | +1.489 | +0.965 |
| Al(13) | +1.994 | +0.678 | +1.527 | +0.992 |  | +2.022 | +0.681 | +1.545 | +0.973 |  | +1.995 | +0.654 | +1.466 | +0.966 |
| O(14) | −1.204 | −0.437 | −1.122 | −0.664 |  | −1.217 | −0.444 | −1.106 | −0.653 |  | −1.219 | −0.447 | −1.041 | −0.653 |
| O(15) | −1.204 | −0.437 | −1.122 | −0.664 |  | −1.217 | −0.444 | −1.106 | −0.653 |  | −1.224 | −0.449 | −1.057 | −0.652 |
| O(16) | −1.111 | −0.402 | −0.904 | −0.700 |  | −1.118 | −0.403 | −0.917 | −0.704 |  | −1.113 | −0.393 | −0.912 | −0.694 |
| O(17) | −1.111 | −0.402 | −0.904 | −0.700 |  | −1.118 | −0.403 | −0.917 | −0.704 |  | −1.111 | −0.391 | −0.907 | −0.693 |
| O(18) | −1.266 | −0.442 | −1.031 | −0.691 |  | −1.262 | −0.353 | −1.012 | −0.707 |  | −1.256 | −0.347 | −1.729 | −0.695 |
| O(19) | −1.192 | −0.428 | −1.045 | −0.655 |  | −1.207 | −0.452 | −0.968 | −0.675 |  | −1.243 | −0.412 | −0.863 | −0.703 |
| O(20) | −1.192 | −0.428 | −1.045 | −0.655 |  | −1.207 | −0.452 | −0.968 | −0.675 |  | −1.237 | −0.408 | −0.775 | −0.717 |
| O(21) | −1.407 | −0.383 | −1.008 | −0.775 |  | −1.434 | −0.388 | −0.984 | −0.770 |  | −1.445 | −0.392 | −0.982 | −0.776 |
| O(22) | −1.407 | −0.383 | −1.008 | −0.775 |  | −1.434 | −0.388 | −0.984 | −0.770 |  | −1.447 | −0.391 | −0.933 | −0.776 |
| O(23) | −1.095 | −0.401 | −1.027 | −0.603 |  | −1.090 | −0.402 | −0.969 | −0.588 |  | −1.140 | −0.432 | −1.002 | −0.625 |
| O(24) | −1.095 | −0.401 | −1.027 | −0.603 |  | −1.090 | −0.402 | −0.969 | −0.588 |  | −1.132 | −0.426 | −0.977 | −0.618 |
| O(25) | −1.291 | −0.366 | −0.852 | −0.742 |  | −1.306 | −0.323 | −0.953 | −0.780 |  | −1.324 | −0.333 | −0.496 | −0.792 |
| O(26) | −1.292 | −0.369 | −0.967 | −0.713 |  | −1.280 | −0.372 | −0.877 | −0.687 |  | −1.284 | −0.371 | −0.832 | −0.686 |
| O(27) | −1.292 | −0.369 | −0.967 | −0.713 |  | −1.280 | −0.372 | −0.877 | −0.687 |  | −1.289 | −0.375 | −0.864 | −0.688 |
| O(28) | −1.386 | −0.383 | −0.964 | −0.778 |  | -1.398 | −0.383 | −0.930 | −0.759 |  | −1.387 | −0.383 | −0.951 | −0.753 |
| O(29) | −1.386 | −0.383 | −0.964 | −0.778 |  | −1.398 | −0.383 | −0.930 | −0.759 |  | −1.386 | −0.383 | −0.917 | −0.753 |
| O(30) | −1.277 | −0.473 | -1.003 | −0.686 |  | −1.281 | −0.475 | −1.023 | −0.677 |  | −1.281 | −0.476 | −1.022 | −0.674 |
| O(31) | −1.277 | −0.473 | −1.003 | −0.686 |  | −1.281 | −0.475 | −1.023 | −0.677 |  | −1.280 | −0.477 | −1.005 | −0.672 |
| O(32) | −1.118 | −0.388 | −0.899 | −0.702 |  | −1.124 | −0.389 | −0.911 | −0.704 |  | −1.126 | −0.391 | −0.896 | −0.706 |
| O(33) | −1.118 | −0.388 | −0.899 | −0.702 |  | −1.124 | −0.389 | −0.911 | −0.704 |  | −1.128 | −0.393 | −0.904 | −0.708 |
| H(34) | +0.481 | +0.159 | +0.422 | +0.399 |  | +0.483 | +0.159 | +0.426 | +0.407 |  | +0.487 | +0.163 | +0.426 | +0.412 |
| H(35) | +0.481 | +0.159 | +0.422 | +0.399 |  | +0.483 | +0.159 | +0.426 | +0.407 |  | +0.487 | +0.164 | +0.423 | +0.412 |
| H(36) | +0.506 | +0.181 | +0.422 | +0.428 |  | +0.506 | +0.181 | +0.429 | +0.435 |  | +0.503 | +0.179 | +0.426 | +0.432 |
| H(37) | +0.506 | +0.181 | +0.422 | +0.428 |  | +0.506 | +0.181 | +0.429 | +0.435 |  | +0.503 | +0.178 | +0.428 | +0.431 |
| O(38) | −1.068 | −0.421 | −1.003 | −0.720 |  | −1.062 | −0.415 | −0.981 | −0.713 |  | −1.055 | −0.410 | −0.943 | −0.700 |
| O(39) | −1.159 | −0.284 | −0.790 | −0.763 |  | −1.167 | −0.280 | −0.741 | −0.762 |  | −1.168 | −0.284 | −0.806 | −0.763 |
| O(40) | −1.098 | −0.395 | −0.930 | −0.743 |  | −1.103 | −0.399 | −0.908 | −0.738 |  | −1.104 | −0.403 | −0.932 | −0.735 |
| H(41) | +0.489 | +0.144 | +0.588 | +0.416 |  | +0.492 | +0.147 | +0.574 | +0.434 |  | +0.492 | +0.147 | +0.538 | +0.440 |
| H(42) | +0.530 | +0.188 | +0.458 | +0.474 |  | +0.533 | +0.190 | +0.438 | +0.483 |  | +0.536 | +0.189 | +0.496 | +0.486 |
| H(43) | +0.495 | +0.158 | +0.429 | +0.432 |  | +0.490 | +0.154 | +0.415 | +0.432 |  | +0.488 | +0.152 | +0.440 | +0.430 |
| Pd(1) |  |  |  |  |  | +0.173 | +0.243 | +0.105 | +0.116 |  | +0.139 | +0.239 | +0.054 | −0.083 |
| Pd(2) |  |  |  |  |  | +0.045 | +0.137 | −0.157 | +0.017 |  | +0.043 | +0.063 | +0.085 | −0.224 |
| Pd(3) |  |  |  |  |  | +0.040 | +0.096 | +0.136 | −0.232 |  | +0.233 | +0.251 | +0.235 | −0.184 |
| Pd(4) |  |  |  |  |  | +0.040 | +0.096 | +0.136 | −0.232 |  | −0.033 | +0.112 | −0.377 | −0.115 |
| Pd(5) |  |  |  |  |  |  |  |  |  |  | +0.041 | −0.043 | +0.130 | +0.005 |

Table S4 Bond distance (d) and bond angle (a) in Pd4 clusters with planar (in D2h symmetry, single point) and tetrahedral (in Cs, resulting from the optimization of the isolated planar form, and Td, single point, symmetries) arrangements

| Arrangement | Planar | Tetrahedral |  |
| --- | --- | --- | --- |
| Symmetry | D2h | Cs | Td |
| da (Å) | 2.751 4.765(3–3†) | 2.605(1–2) 2.712(1–3) 2.604(2–3) 2.717(3–3†) | 2.751 |
| aa (°) | 60.00 | 62.75(1–2–3) 58.64(1–3–2) 58.61(2–1–3) | 60.00 |

a Palladium atoms involved (1, 2, 3 or 3† (symmetric to Pd(3)).

Table S5 Bonding energy of each palladium atom in: Pd4/Al13O23H7 complex (Eb(Pd4/sup)) and boat Pd4 (Eb(Pd4)) and γ-alumina (Eb(sup)) moieties

| Pd | (1) | (2) | (3) |
| --- | --- | --- | --- |
| Site | Odi | Otr | Alo |
| Eb(Pd4/sup) (kcal mol-1) | −65.03 | −47.49 | −48.48 |
| Eb(Pd4) (kcal mol-1) | −54.77 | −54.53 | −33.42 |
| Eb(sup) (kcal mol-1) | −34.08 | −21.89 | −24.74 |

Table S6 Charge distribution (q) in the Pd1(sp)/Al13O23H7 complexes calculated with NBO, Hirshfeld, Merz-Singh-Kollman, and Mulliken methods

| Model | NBO |  |  |  | Hirshfeld |  |  |  | Merz-Singh-Kollman |  |  |  | Mulliken |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom/q (ē) | Pd(1) | Pd(2) | Pd(3) |  | Pd(1) | Pd(2) | Pd(3) |  | Pd(1) | Pd(2) | Pd(3) |  | Pd(1) | Pd(2) | Pd(3) |
| Al(1) | +1.951 | +1.985 | +1.978 |  | +0.650 | +0.699 | +0.692 |  | +1.792 | +1.706 | +1.701 |  | +1.141 | +1.101 | +1.091 |
| Al(2) | +1.930 | +1.932 | +1.923 |  | +0.601 | +0.618 | +0.609 |  | +1.614 | +1.602 | +1.622 |  | +0.903 | +0.934 | +0.918 |
| Al(3) | +1.930 | +1.932 | +1.927 |  | +0.601 | +0.618 | +0.614 |  | +1.614 | +1.602 | +1.599 |  | +0.903 | +0.934 | +0.929 |
| Al(4) | +2.020 | +2.016 | +2.016 |  | +0.674 | +0.666 | +0.670 |  | +1.797 | +1.616 | +1.614 |  | +1.105 | +0.968 | +0.987 |
| Al(5) | +1.856 | +1.892 | +1.915 |  | +0.560 | +0.590 | +0.624 |  | +1.519 | +1.588 | +1.637 |  | +1.127 | +1.089 | +1.072 |
| Al(6) | +1.856 | +1.892 | +1.659 |  | +0.560 | +0.590 | +0.398 |  | +1.519 | +1.588 | +1.214 |  | +1.127 | +1.089 | +1.044 |
| Al(7) | +1.791 | +1.796 | +1.789 |  | +0.483 | +0.486 | +0.487 |  | +0.991 | +1.023 | +1.072 |  | +1.035 | +1.124 | +1.049 |
| Al(8) | +1.791 | +1.796 | +1.796 |  | +0.483 | +0.486 | +0.485 |  | +0.991 | +1.023 | +1.102 |  | +1.035 | +1.124 | +1.088 |
| Al(9) | +1.692 | +1.690 | +1.689 |  | +0.609 | +0.605 | +0.612 |  | +1.351 | +1.310 | +1.326 |  | +0.888 | +0.885 | +0.898 |
| Al(10) | +1.692 | +1.690 | +1.704 |  | +0.609 | +0.605 | +0.615 |  | +1.351 | +1.310 | +1.358 |  | +0.888 | +0.885 | +0.903 |
| Al(11) | +1.907 | +1.783 | +1.904 |  | +0.643 | +0.552 | +0.640 |  | +1.526 | +1.376 | +1.522 |  | +0.964 | +0.972 | +0.962 |
| Al(12) | +1.983 | +1.995 | +1.987 |  | +0.648 | +0.652 | +0.651 |  | +1.463 | +1.486 | +1.470 |  | +0.943 | +0.946 | +0.942 |
| Al(13) | +1.983 | +1.995 | +1.984 |  | +0.648 | +0.652 | +0.650 |  | +1.463 | +1.486 | +1.463 |  | +0.943 | +0.946 | +0.950 |
| O(14) | −1.168 | −1.134 | −1.147 |  | −0.409 | −0.389 | −0.397 |  | −1.032 | −1.034 | −1.055 |  | −0.631 | −0.619 | -0.637 |
| O(15) | −1.168 | −1.134 | −1.143 |  | −0.409 | −0.389 | −0.394 |  | −1.032 | −1.034 | −1.031 |  | −0.631 | −0.619 | −0.610 |
| O(16) | −1.119 | −1.116 | −1.114 |  | −0.398 | −0.395 | −0.395 |  | −0.923 | −0.906 | −0.920 |  | −0.703 | −0.705 | −0.699 |
| O(17) | −1.119 | −1.116 | −1.117 |  | −0.398 | −0.395 | −0.396 |  | −0.923 | −0.906 | −0.905 |  | −0.703 | −0.705 | −0.702 |
| O(18) | −1.242 | −1.162 | −1.154 |  | −0.320 | −0.377 | −0.371 |  | −1.421 | −0.861 | −0.861 |  | −0.676 | −0.612 | −0.622 |
| O(19) | −1.250 | −1.235 | −1.236 |  | −0.466 | −0.451 | −0.452 |  | −1.035 | −1.065 | −1.098 |  | −0.685 | −0.686 | −0.674 |
| O(20) | −1.250 | −1.235 | −1.193 |  | −0.466 | −0.451 | −0.439 |  | −1.035 | −1.065 | −1.007 |  | −0.685 | −0.686 | −0.659 |
| O(21) | −1.428 | −1.421 | −1.416 |  | −0.389 | −0.388 | −0.387 |  | −1.013 | −0.992 | −1.011 |  | −0.763 | −0.767 | −0.755 |
| O(22) | −1.428 | −1.421 | −1.409 |  | −0.389 | −0.388 | −0.388 |  | −1.013 | −0.992 | −0.992 |  | −0.763 | −0.767 | −0.760 |
| O(23) | −1.134 | −1.142 | −1.135 |  | −0.429 | −0.434 | −0.430 |  | −1.036 | −1.038 | −1.054 |  | −0.619 | −0.628 | −0.614 |
| O(24) | −1.134 | −1.142 | −1.127 |  | −0.429 | −0.434 | −0.429 |  | −1.036 | −1.038 | −0.992 |  | −0.619 | −0.628 | −0.620 |
| O(25) | −1.303 | −1.333 | −1.301 |  | −0.383 | −0.326 | −0.378 |  | −0.890 | −1.268 | −0.890 |  | −0.724 | −0.776 | −0.724 |
| O(26) | −1.294 | −1.294 | −1.278 |  | −0.372 | −0.372 | −0.371 |  | −0.930 | −0.911 | −0.912 |  | −0.685 | −0.683 | −0.682 |
| O(27) | −1.294 | −1.294 | −1.292 |  | −0.372 | −0.372 | −0.370 |  | −0.930 | −0.911 | −0.958 |  | −0.685 | −0.683 | −0.682 |
| O(28) | −1.389 | −1.393 | −1.391 |  | −0.385 | −0.383 | −0.386 |  | −0.898 | −0.809 | −0.952 |  | −0.755 | −0.754 | −0.757 |
| O(29) | −1.389 | −1.393 | −1.388 |  | −0.385 | −0.383 | −0.384 |  | −0.898 | −0.809 | −0.925 |  | −0.755 | −0.754 | −0.754 |
| O(30) | −1.281 | −1.281 | −1.283 |  | −0.479 | −0.479 | −0.480 |  | −1.008 | −1.005 | −1.016 |  | −0.677 | −0.668 | −0.675 |
| O(31) | −1.281 | −1.281 | −1.280 |  | −0.479 | −0.479 | −0.478 |  | −1.008 | −1.005 | −1.002 |  | −0.677 | −0.668 | −0.675 |
| O(32) | −1.127 | −1.128 | −1.127 |  | −0.394 | −0.394 | −0.394 |  | −0.899 | −0.931 | −0.900 |  | −0.710 | −0.711 | −0.710 |
| O(33) | −1.127 | −1.128 | −1.127 |  | −0.394 | −0.394 | −0.393 |  | −0.899 | −0.931 | −0.899 |  | −0.710 | −0.711 | −0.707 |
| H(34) | +0.491 | +0.494 | +0.492 |  | +0.167 | +0.170 | +0.168 |  | +0.434 | +0.432 | +0.440 |  | +0.417 | +0.418 | +0.416 |
| H(35) | +0.491 | +0.494 | +0.492 |  | +0.167 | +0.170 | +0.168 |  | +0.434 | +0.432 | +0.434 |  | +0.417 | +0.418 | +0.416 |
| H(36) | +0.501 | +0.502 | +0.501 |  | +0.177 | +0.177 | +0.177 |  | +0.421 | +0.433 | +0.425 |  | +0.429 | +0.430 | +0.429 |
| H(37) | +0.501 | +0.502 | +0.501 |  | +0.177 | +0.177 | +0.177 |  | +0.421 | +0.433 | +0.424 |  | +0.429 | +0.430 | +0.429 |
| O(38) | −1.004 | −0.985 | −0.996 |  | −0.370 | −0.354 | −0.363 |  | −0.914 | −0.874 | −0.883 |  | −0.666 | −0.627 | −0.673 |
| O(39) | −1.166 | −1.169 | −1.166 |  | −0.289 | −0.286 | −0.289 |  | −0.767 | −0.683 | −0.819 |  | −0.761 | −0.761 | −0.761 |
| O(40) | −1.103 | −1.105 | −1.103 |  | −0.404 | −0.407 | −0.405 |  | −0.959 | −0.951 | −0.952 |  | −0.746 | −0.736 | −0.748 |
| H(41) | +0.495 | +0.496 | +0.495 |  | +0.156 | +0.158 | +0.157 |  | +0.554 | +0.548 | +0.545 |  | +0.442 | +0.439 | +0.436 |
| H(42) | +0.532 | +0.535 | +0.531 |  | +0.187 | +0.189 | +0.186 |  | +0.463 | +0.410 | +0.475 |  | +0.481 | +0.483 | +0.480 |
| H(43) | +0.490 | +0.484 | +0.490 |  | +0.154 | +0.149 | +0.153 |  | +0.437 | +0.437 | +0.442 |  | +0.431 | +0.425 | +0.432 |
| Pd(1) | +0.315 |  |  |  | +0.258 |  |  |  | +0.347 |  |  |  | −0.021 |  |  |
| Pd(2) |  | +0.140 |  |  |  | +0.120 |  |  |  | +0.171 |  |  |  | −0.086 |  |
| Pd(3) |  |  | +0.148 |  |  |  | +0.238 |  |  |  | +0.148 |  |  |  | +0.030 |

Table S7 Bond distances (d) in Pd5/Al13O23H7 complex

| Pair | Distance |
| --- | --- |
| dPd−Pda(Å) | 3.191(1–2) 2.728(1–3) 2.966(1–4) 2.656(1–5) 2.667(2–3) 2.790(2–4) 2.601(2–5) 4.514(3–4) 2.928(3–5) 2.758(4–5) |
| dPd−Ala (Å) | 2.575(3–Alo) 2.638(4–Alo) |
| dPd−Oa(Å) | 2.233(1–Odi) 2.110(1–Odi*) 2.143(2–Otr) 2.902(3–Otr*) 2.246(4–Odi) 2.160(4–Odi*) |

a Pd−Pd and Pd−ion pairs.

Table S8 Charge distribution (q) on the palladium atoms in the isolated Pd4 and Pd5 clusters (obtained in the presence of γ-alumina) calculated with the NBO, Hirshfeld (Hirsh.), Merz-Singh-Kollman (MSK), and Mulliken (Mul.) methods

| Cluster | Pd4 |  |  |  |  | Pd5 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom/q (ē) | NBO | Hirsh. | MSK | Mul. |  | NBO | Hirsh. | MSK | Mul. |
| Pd(1) | −0.152 | −0.017 | −0.122 | +0.006 |  | +0.024 | +0.011 | −0.038 | +0.050 |
| Pd(2) | −0.147 | −0.019 | −0.115 | +0.006 |  | +0.055 | −0.021 | +0.069 | −0.024 |
| Pd(3) | +0.150 | +0.018 | +0.118 | −0.006 |  | +0.092 | −0.014 | +0.074 | −0.005 |
| Pd(4) | +0.150 | +0.018 | +0.118 | −0.006 |  | −0.048 | +0.001 | −0.061 | +0.045 |
| Pd(5) |  |  |  |  |  | −0.123 | +0.023 | −0.045 | −0.066 |

Table S9 Relative energy (Erel) and spin contamination (S2 and S2(A), A=annihilated) calculated for the NO/Pd4/Al13O23H7 and NO/Pd4(boat) clusters in different electronic spin states (ESS) with the B3LYP functional and the 6-311+G(d)/LANL2DZ/6-31G(d) and 6-311+G(d)/LANL2DZ basis sets, respectively

| Structure | Site | ESS | S | S2 | S2 (A) | Erel (kcal mol-1) |
| --- | --- | --- | --- | --- | --- | --- |
| NO/Pd4/γ-alumina | Pd(1) | Duplet | 0.50 | 0.99 | 0.77 | 0.00 |
|  |  | Quartet | 0.75 | 3.81 | 3.75 | 14.16 |
|  | Pd(2) | Duplet | 0.50 | 0.94 | 0.76 | 0.00 |
|  |  | Quartet | 0.75 | 3.80 | 3.75 | 11.44 |
|  | Pd(3) | Duplet | 0.50 | 1.65 | 0.91 | 0.00 |
|  |  | Quartet | 0.75 | 3.80 | 3.75 | 1.50 |
|  | Pd(1)−(2) | Duplet | 0.50 | 0.78 | 0.75 | 0.00 |
|  |  | Quartet | 0.75 | 3.79 | 3.75 | 13.48 |
| NO/Pd4 | Pd(1) | Duplet | 0.50 | 1.05 | 0.77 | 0.00 |
|  |  | Quartet | 0.75 | 3.81 | 3.75 | 7.76 |
|  | Pd(2) | Duplet | 0.50 | 1.05 | 0.77 | 0.00 |
|  |  | Quartet | 0.75 | 3.81 | 3.75 | 7.72 |
|  | Pd(3) | Duplet | 0.50 | 0.80 | 0.75 | 0.00 |
|  |  | Quartet | 0.75 | 3.78 | 3.75 | 12.44 |
|  | Pd(1)−(2) | Duplet | 0.50 | 0.78 | 0.75 | 0.00 |
|  |  | Quartet | 0.75 | 3.80 | 3.75 | 20.88 |

Table S10 Charge distribution (q) in the NO/Pd4/Al13O23H7 complexes calculated with NBO, Hirshfeld, Merz-Singh-Kollman, and Mulliken methods

| Model | NBO |  |  |  |  | Hirshfeld |  |  |  |  | Merz-Singh-Kollman |  |  |  |  | Mulliken |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pd site/q (ē) | (1) | (2) | (3) | (1)−(2) |  | (1) | (2) | (3) | (1)−(2) |  | (1) | (2) | (3) | (1)−(2) |  | (1) | (2) | (3) | (1)−(2) |
| Al(1) | +1.960 | +1.953 | +1.958 | +1.961 |  | +0.619 | +0.622 | +0.627 | +0.623 |  | +1.775 | +1.762 | +1.811 | +1.783 |  | +1.108 | +1.087 | +1.103 | +1.085 |
| Al(2) | +1.904 | +1.905 | +1.912 | +1.904 |  | +0.564 | +0.565 | +0.568 | +0.566 |  | +1.613 | +1.586 | +1.565 | +1.550 |  | +0.876 | +0.872 | +0.869 | +0.873 |
| Al(3) | +1.904 | +1.905 | +1.907 | +1.903 |  | +0.564 | +0.565 | +0.569 | +0.566 |  | +1.597 | +1.587 | +1.592 | +1.555 |  | +0.873 | +0.877 | +0.879 | +0.872 |
| Al(4) | +2.065 | +2.059 | +2.061 | +2.062 |  | +0.673 | +0.675 | +0.678 | +0.676 |  | +1.824 | +1.707 | +1.801 | +1.747 |  | +1.055 | +1.061 | +1.061 | +1.068 |
| Al(5) | +1.694 | +1.685 | +1.688 | +1.699 |  | +0.374 | +0.373 | +0.379 | +0.378 |  | +1.179 | +1.136 | +1.260 | +1.256 |  | +1.258 | +1.248 | +1.240 | +1.231 |
| Al(6) | +1.704 | +1.691 | +1.712 | +1.705 |  | +0.377 | +0.375 | +0.370 | +0.381 |  | +1.192 | +1.154 | +1.335 | +1.213 |  | +1.272 | +1.247 | +1.287 | +1.232 |
| Al(7) | +1.880 | +1.881 | +1.877 | +1.875 |  | +0.512 | +0.511 | +0.514 | +0.513 |  | +1.217 | +1.204 | +1.229 | +1.240 |  | +1.157 | +1.157 | +1.147 | +1.145 |
| Al(8) | +1.880 | +1.881 | +1.884 | +1.876 |  | +0.512 | +0.512 | +0.513 | +0.513 |  | +1.235 | +1.204 | +1.197 | +1.241 |  | +1.156 | +1.155 | +1.159 | +1.144 |
| Al(9) | +1.748 | +1.747 | +1.749 | +1.746 |  | +0.648 | +0.647 | +0.650 | +0.646 |  | +1.388 | +1.385 | +1.382 | +1.373 |  | +0.913 | +0.921 | +0.925 | +0.917 |
| Al(10) | +1.749 | +1.748 | +1.762 | +1.748 |  | +0.649 | +0.648 | +0.647 | +0.649 |  | +1.381 | +1.391 | +1.389 | +1.378 |  | +0.910 | +0.930 | +0.924 | +0.919 |
| Al(11) | +1.867 | +1.915 | +1.854 | +1.893 |  | +0.571 | +0.596 | +0.572 | +0.592 |  | +1.564 | +1.611 | +1.427 | +1.558 |  | +0.966 | +1.013 | +0.978 | +0.988 |
| Al(12) | +2.021 | +2.021 | +2.019 | +2.017 |  | +0.681 | +0.681 | +0.683 | +0.682 |  | +1.547 | +1.545 | +1.545 | +1.535 |  | +0.974 | +0.983 | +0.976 | +0.973 |
| Al(13) | +2.021 | +2.021 | +2.018 | +2.016 |  | +0.681 | +0.680 | +0.683 | +0.681 |  | +1.541 | +1.544 | +1.554 | +1.535 |  | +0.972 | +0.979 | +0.974 | +0.972 |
| O(14) | −1.217 | −1.213 | −1.203 | −1.211 |  | −0.444 | −0.442 | −0.434 | -0.440 |  | −1.087 | −1.098 | −1.059 | −1.080 |  | −0.650 | −0.642 | −0.647 | −0.646 |
| O(15) | −1.221 | −1.213 | −1.200 | −1.212 |  | −0.446 | −0.442 | −0.432 | −0.441 |  | −1.084 | −1.097 | −1.073 | −1.081 |  | −0.659 | −0.654 | −0.648 | −0.644 |
| O(16) | −1.118 | −1.118 | −1.119 | −1.118 |  | −0.403 | −0.403 | −0.403 | −0.403 |  | −0.942 | −0.933 | −0.925 | −0.917 |  | −0.704 | −0.704 | −0.705 | −0.700 |
| O(17) | −1.118 | −1.118 | −1.119 | −1.118 |  | −0.404 | −0.404 | −0.404 | −0.403 |  | −0.941 | −0.934 | −0.924 | −0.916 |  | −0.705 | −0.705 | −0.702 | −0.701 |
| O(18) | −1.279 | −1.255 | −1.218 | −1.284 |  | −0.373 | −0.348 | −0.332 | −0.373 |  | −1.581 | −1.235 | −1.460 | −1.282 |  | −0.731 | −0.702 | −0.690 | −0.722 |
| O(19) | −1.207 | −1.208 | −1.214 | −1.202 |  | −0.454 | −0.453 | −0.455 | −0.449 |  | −0.944 | −0.952 | −0.985 | −0.970 |  | −0.679 | −0.682 | −0.683 | −0.664 |
| O(20) | −1.206 | −1.207 | −1.226 | −1.201 |  | −0.452 | −0.452 | −0.460 | −0.448 |  | −0.974 | −0.949 | −0.964 | −0.951 |  | −0.674 | −0.678 | −0.679 | −0.665 |
| O(21) | −1.433 | −1.433 | −1.433 | −1.431 |  | −0.388 | −0.388 | −0.388 | −0.387 |  | −0.988 | −0.977 | −1.027 | −1.031 |  | −0.771 | −0.771 | −0.772 | −0.769 |
| O(22) | −1.433 | −1.433 | −1.436 | −1.431 |  | −0.388 | −0.388 | −0.388 | −0.387 |  | −1.008 | −0.978 | −1.019 | −1.018 |  | −0.771 | −0.772 | −0.770 | −0.768 |
| O(23) | −1.090 | −1.089 | −1.090 | −1.090 |  | −0.402 | −0.402 | −0.402 | −0.402 |  | −0.961 | −0.957 | −0.963 | −0.962 |  | −0.587 | −0.585 | −0.593 | −0.582 |
| O(24) | −1.089 | −1.089 | −1.099 | −1.089 |  | −0.402 | −0.402 | −0.403 | −0.402 |  | −0.952 | −0.960 | −0.991 | −0.956 |  | −0.583 | −0.593 | −0.576 | −0.585 |
| O(25) | −1.305 | −1.300 | −1.299 | −1.293 |  | −0.323 | −0.332 | −0.319 | −0.323 |  | −1.327 | −0.977 | −1.105 | −1.118 |  | −0.778 | −0.789 | −0.780 | −0.782 |
| O(26) | −1.277 | −1.279 | −1.283 | −1.277 |  | −0.371 | −0.373 | −0.373 | −0.372 |  | −0.848 | −0.850 | −0.852 | −0.872 |  | −0.686 | −0.688 | −0.696 | −0.688 |
| O(27) | −1.278 | −1.279 | −1.278 | −1.277 |  | −0.371 | −0.373 | −0.371 | −0.372 |  | −0.838 | −0.832 | −0.898 | −0.883 |  | −0.688 | −0.687 | −0.686 | −0.689 |
| O(28) | −1.396 | −1.397 | −1.386 | −1.385 |  | −0.383 | −0.383 | −0.383 | −0.383 |  | −0.934 | −0.987 | −0.903 | −0.951 |  | −0.759 | −0.762 | −0.761 | −0.756 |
| O(29) | −1.396 | −1.398 | −1.386 | −1.385 |  | −0.383 | −0.383 | −0.383 | −0.383 |  | −0.943 | −0.988 | −0.937 | −0.945 |  | −0.759 | −0.761 | −0.759 | −0.757 |
| O(30) | −1.281 | −1.281 | −1.283 | −1.281 |  | −0.475 | −0.475 | −0.475 | −0.475 |  | −1.025 | −1.024 | −1.032 | −1.020 |  | −0.679 | −0.682 | −0.675 | −0.677 |
| O(31) | −1.281 | −1.281 | −1.282 | −1.281 |  | −0.476 | −0.476 | −0.475 | −0.475 |  | −1.028 | −1.025 | −1.021 | −1.020 |  | −0.681 | −0.679 | −0.677 | −0.676 |
| O(32) | −1.124 | −1.124 | −1.125 | −1.124 |  | −0.389 | −0.388 | −0.389 | −0.388 |  | −0.924 | −0.905 | −0.931 | −0.913 |  | −0.705 | −0.704 | −0.706 | −0.702 |
| O(33) | −1.124 | −1.124 | −1.124 | −1.124 |  | −0.389 | −0.389 | −0.389 | −0.389 |  | −0.915 | −0.905 | −0.914 | −0.914 |  | −0.705 | −0.706 | −0.704 | −0.704 |
| H(34) | +0.483 | +0.483 | +0.485 | +0.483 |  | +0.159 | +0.159 | +0.161 | +0.159 |  | +0.434 | +0.429 | +0.431 | +0.427 |  | +0.406 | +0.407 | +0.409 | +0.406 |
| H(35) | +0.483 | +0.483 | +0.485 | +0.483 |  | +0.159 | +0.159 | +0.160 | +0.159 |  | +0.432 | +0.430 | +0.426 | +0.425 |  | +0.406 | +0.407 | +0.408 | +0.406 |
| H(36) | +0.506 | +0.506 | +0.506 | +0.506 |  | +0.181 | +0.181 | +0.181 | +0.181 |  | +0.437 | +0.428 | +0.443 | +0.436 |  | +0.435 | +0.436 | +0.435 | +0.435 |
| H(37) | +0.506 | +0.506 | +0.506 | +0.506 |  | +0.181 | +0.181 | +0.181 | +0.181 |  | +0.435 | +0.428 | +0.431 | +0.436 |  | +0.435 | +0.436 | +0.435 | +0.435 |
| O(38) | −1.063 | −1.061 | −1.061 | -1.061 |  | −0.415 | −0.415 | −0.413 | −0.414 |  | −0.968 | −0.972 | −0.976 | −0.974 |  | −0.723 | −0.712 | −0.711 | −0.705 |
| O(39) | −1.167 | −1.167 | −1.166 | −1.166 |  | −0.280 | −0.280 | −0.280 | −0.279 |  | −0.773 | −0.818 | −0.791 | −0.777 |  | −0.763 | −0.764 | −0.765 | −0.763 |
| O(40) | −1.102 | −1.104 | −1.101 | −1.101 |  | −0.400 | −0.397 | −0.400 | −0.397 |  | −0.941 | −0.940 | −0.918 | −0.920 |  | −0.739 | −0.737 | −0.739 | −0.737 |
| H(41) | +0.493 | +0.492 | +0.491 | +0.492 |  | +0.147 | +0.147 | +0.147 | +0.147 |  | +0.566 | +0.570 | +0.562 | +0.562 |  | +0.438 | +0.434 | +0.434 | +0.434 |
| H(42) | +0.533 | +0.533 | +0.534 | +0.534 |  | +0.190 | +0.190 | +0.190 | +0.190 |  | +0.461 | +0.482 | +0.460 | +0.447 |  | +0.483 | +0.483 | +0.484 | +0.484 |
| H(43) | +0.488 | +0.492 | +0.488 | +0.492 |  | +0.153 | +0.155 | +0.153 | +0.155 |  | +0.434 | +0.430 | +0.425 | +0.419 |  | +0.431 | +0.435 | +0.430 | +0.435 |
| Pd(1) | +0.053 | +0.236 | +0.168 | +0.238 |  | +0.310 | +0.242 | +0.214 | +0.282 |  | +0.583 | +0.201 | +0.315 | +0.202 |  | −0.136 | +0.147 | +0.030 | +0.251 |
| Pd(2) | +0.100 | −0.077 | +0.081 | +0.123 |  | +0.126 | +0.200 | +0.104 | +0.170 |  | −0.054 | −0.330 | +0.022 | −0.106 |  | +0.080 | −0.152 | +0.004 | +0.045 |
| Pd(3) | +0.082 | +0.058 | −0.030 | +0.130 |  | +0.122 | +0.098 | +0.130 | +0.159 |  | +0.134 | +0.188 | −0.017 | +0.157 |  | −0.226 | −0.237 | −0.203 | −0.184 |
| Pd(4) | +0.081 | +0.066 | +0.052 | +0.118 |  | +0.120 | +0.105 | +0.104 | +0.149 |  | +0.123 | +0.202 | +0.110 | +0.143 |  | −0.210 | −0.222 | −0.223 | −0.192 |
| N | +0.155 | +0.148 | +0.122 | −0.154 |  | +0.003 | −0.006 | +0.018 | −0.068 |  | −0.070 | +0.086 | +0.058 | +0.210 |  | +0.018 | −0.012 | −0.076 | −0.308 |
| O | −0.158 | −0.169 | −0.161 | −0.216 |  | −0.064 | −0.073 | −0.044 | −0.147 |  | −0.041 | −0.070 | −0.082 | −0.251 |  | +0.126 | +0.065 | +0.032 | +0.016 |

Table S11 Adsorption energy (Ead) for NO molecule on isolated boat Pd4 clusters, in bridge and hollow modes, geometric parameters (bond distance (d) and bond angle (a)) and NBO charge (q) on γ-alumina, Pd4, Pd atom bonded to NO and NO moieties

| Mode | Bridge |  |  | Hollow |  |
| --- | --- | --- | --- | --- | --- |
| Pd site | (1)−(3) | (2)−(3) |  | (1)−(2)−(3) |  |
| Eads (kcal mol-1) | ‒39.18 | ‒39.24 |  | ‒33.36 |  |
| dPd–Na (Å) | 1.965(1) 1.983(3) | 1.965(2) 1.984(3) |  | 1.993(1) 1.993(2) 2.012(3) |  |
| dN–Oa (Å) | 1.180 | 1.180 |  | 1.206 |  |
| aPd–N–Oa (°) | 124.69(1) 121.12(3) | 124.37(2) 120.89(3) |  | 127.03(1) 126.86(2) 126.48(3) |  |
| qPd4 (ē) | +0.188 | +0.190 |  | +0.441 |  |
| qPda (ē) | +0.003(1) +0.217(3) | +0.009(2) +0.217(3) |  | +0.136(1) +0.139(2) +0.171(3) |  |
| qNO (ē) | ‒0.188 | ‒0.190 |  | ‒0.441 |  |

a Palladium atom at the adsorption site (1, 2, or 3).

Table S12 Charge distribution (q) in the NO/Pd4(boat) agglomerates, calculated with NBO, Hirshfeld, Merz-Singh-Kollman, and Mulliken methods

| Model | NBO |  |  |  |  | Hirshfeld |  |  |  |  | Merz-Singh-Kollman |  |  |  |  | Mulliken |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom/q (ē) | (1) | (2) | (3) | (1)−(2) |  | (1) | (2) | (3) | (1)−(2) |  | (1) | (2) | (3) | (1)−(2) |  | (1) | (2) | (3) | (1)−(2) |
| Pd(1) | −0.157 | −0.122 | −0.126 | +0.165 |  | +0.084 | −0.043 | −0.055 | +0.111 |  | −0.308 | −0.072 | −0.048 | +0.035 |  | +0.239 | −0.029 | −0.028 | +0.150 |
| Pd(2) | −0.116 | −0.151 | −0.117 | +0.167 |  | −0.042 | +0.085 | −0.054 | +0.112 |  | −0.068 | −0.304 | −0.047 | +0.036 |  | −0.029 | +0.237 | −0.029 | +0.152 |
| Pd(3) | +0.118 | +0.119 | +0.086 | +0.068 |  | −0.017 | −0.017 | +0.105 | −0.002 |  | +0.138 | +0.139 | −0.079 | +0.059 |  | −0.054 | −0.055 | +0.206 | −0.012 |
| Pd(4) | +0.173 | +0.173 | +0.146 | +0.068 |  | +0.029 | +0.030 | +0.018 | −0.002 |  | +0.138 | +0.140 | +0.074 | +0.059 |  | −0.029 | −0.030 | −0.037 | −0.012 |
| N | +0.151 | +0.151 | +0.166 | −0.202 |  | +0.015 | +0.016 | +0.036 | −0.041 |  | +0.219 | +0.217 | +0.244 | +0.066 |  | −0.154 | −0.152 | −0.150 | −0.203 |
| O | −0.170 | −0.170 | −0.155 | −0.266 |  | −0.070 | −0.070 | −0.051 | −0.177 |  | −0.119 | −0.119 | −0.144 | −0.255 |  | +0.027 | +0.029 | +0.038 | −0.074 |

To measure the effect of Pd4 distortion on the NO adsorption, the planar and tetrahedral forms (the initial and most stable Pd4 arrangements, respectively) were tested for the interaction with the NO molecule (Fig. S5 (ESI†)). On planar Pd4, the NO adsorption involves energies between −37.6 kcal mol-1 and −50.0 kcal mol-1     (Table S13 (ESI†)). The preferential adsorption mode for NO is in the bridge form on Pd(1)−(3), although, with a value only 1.5 kcal mol-1 higher than that obtained for adsorption in the hollow mode. When adsorbed in the bridge form, NO assumes a charge of −0.191 ē, whereas, for adsorption in the hollow mode, it assumes a higher value, −0.387 ē. As for the tetrahedral arrangement, the ontop and bridge modes present similar adsorption energies (from −26.8 kcal mol-1 to −29.5 kcal mol-1, Table S13 (ESI†)), ontop adsorption on Pd(2) being the highest. Nevertheless, NO assumes the most negative charge in the hollow form (−0.331 ē), the least favored adsorption mode (−15.0 kcal   mol-1).

Fig. S6 Front view of resulting NO/Pd4 agglomerates in planar and tetrahedral arrangements

# Table S13 Adsorption energy (Ead, in kcal mol-1) for NO molecule on isolated Pd4 clusters, in planar and tetrahedral arrangements, geometric parameters (bond distance, in Å, and bond angle, in °) and NBO charge (in ē) on γ-alumina, Pd4, Pd atom bonded to NO and NO moieties

| Cluster | Planar |  |  |  |  |  |  |  |  | Tetrahedral |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mode | Ontop |  |  | Bridge |  |  | Hollow |  |  | Ontop |  |  |  | Bridge |  |  |  | Hollow |
| Site | (1),(2) | (3) |  | (1)−(2) | (1),(2)−(3) |  | (1)−(2)−(3) |  |  | (1) | (2) | (3) |  | (1)−(2) | (1)−(3) | (2)−(3) |  | (1)−(2)−(3) |
| Ead (kcal mol-1) | –38.30 | –40.26 |  | ‒37.56 | ‒49.95 |  | ‒48.48 |  |  | –29.42 | –29.46 | –27.35 |  | ‒26.82 | ‒26.78 | ‒26.80 |  | ‒15.05 |
| dPd−Na (Å) | 1.856 | 1.831 |  | 1.941(1) 1.942(2) | 1.964(1,2) 1.982(3) |  | 1.976(1) 1.976(2) 2.032(3) |  |  | 1.837 | 1.837 | 1.842 |  | 2.025(1) 2.025(2) | 2.014(1) 2.025(3) | 2.010(2) 2.029(3) |  | 2.007(1) 2.006(2) 1.982(3) |
| dN−O (Å) | 1.156 | 1.153 |  | 1.197 | 1.180 |  | 1.200 |  |  | 1.158 | 1.158 | 1.158 |  | 1.191 | 1.189 | 1.190 |  | 1.211 |
| aPd−N−Oa (°) | 129.43 | 134.92 |  | 134.91(1) 134.87(2) | 125.72(1,2) 121.29(3) |  | 125.34(1) 125.18(2) 131.10(3) |  |  | 137.24 | 137.17 | 136.89 |  | 113.12(1) 113.06(2) | 113.67(1) 114.68(3) | 113.65(2) 114.72(3) |  | 129.44(1) 129.44(2) 128.05(3) |
| qPd4 (ē) | ‒0.005 | ‒0.015 |  | +0.400 | +0.191 |  | +0.387 |  |  | +0.011 | +0.013 | +0.012 |  | +0.222 | +0.211 | +0.211 |  | +0.331 |
| qPda (ē) | ‒0.149 | +0.112 |  | +0.145(1) +0.145(2) | ‒0.010(1,2) +0.235(3) |  | +0.110(1) +0.110(2) +0,208(3) |  |  | ‒0.035 | ‒0.036 | ‒0.094 |  | +0.113(1) +0.113(2) | +0.111(1) +0.068(3) | +0.112(2) +0,067(3) |  | +0.192(1) +0.192(2) +0.135(3) |
| qNO (ē) | +0.005 | +0.015 |  | ‒0.400 | ‒0.191 |  | ‒0.387 |  |  | ‒0.011 | ‒0.013 | ‒0.012 |  | ‒0.222 | ‒0.211 | −0.211 |  | −0.331 |

aPalladium atom at the adsorption site (1, 2, or 3)