SCHEMES:

Table 1: Screening of catalysts for the synthesis of benzodiazepinonea

| Entry | Catalyst | Time(hrs) | Yieldb % (3) |
| --- | --- | --- | --- |
| 1. | NaY | 24 | -- |
| 2. | CuY | 24 | 20 |
| 3. | CoY | 24 | 22 |
| 4. | NiY | 24 | 60c |
| 5. | AgY | 10 | 81c |
| 6. | MMZAg(I)Y | 10 | 96 |

aReaction conditions: stirred the mixture of  ortho phenylenediamine (1mmol), methyl acetoacetate (1 mmol),  catalyst (100 mg),  ethanol (3mL) at room temperature for the specified time as mentioned in the table 1 .

bIsolated Yields.

cMinor amount of benzimidazole was also obtained (confirmed by NMR)

Table 2: Synthesis of benzodiazepinone derivativesa

| 3A (96%) | 3B (89%) | 3C (83%) |
| --- | --- | --- |
| 3D (80%) | 3E (76%) | 3F (79%) |
| 3G (78%) | 3H (74%) | 3I (89%) |
| 3J (82%) |  |  |

aReaction conditions: stirred the slurry containing 1,2-diamine compounds(1mmol), β-ketoester / diketone compounds (1 mmol), MMZAgY(100 mg), Ethanol (3mL), at room temperature  for 10hrs.