Supplementary Information for Ultracompact multifunctional metalens visor for augmented reality displays

Yan Li,1 Shuyi Chen,1 Haowen Liang,2 Xiuying Ren,1 Lingcong Luo,2 Yuye Ling,1 Shuxin Liu,1 Yikai Su1 and Shin-Tson Wu3

1Department of Electronic Engineering, Shanghai Jiao Tong University, Shanghai, 200240, China

2State Key Laboratory of Optoelectronic Materials and Technologies, School of Physics, School of Electronics and Information Technology, Sun Yat-Sen University, Guangzhou 510275, China

3College of Optics and Photonics, University of Central Florida, Orlando, FL 32816, USA

*Corresponding authors:

Haowen Liang (lianghw26@mail.sysu.edu.cn)

Yikai Su (yikaisu@sjtu.edu.cn)

Shin-Tson Wu (swu@creol.ucf.edu)

S1.  Phase profile calculation

To focus an oblique incident light as shown in Fig. S1, the secondary waves emerging from each unit on the metalens should arrive at the focal point with the same phase delay to ensure constructive interference. The total phase delay, which is the sum of that imparted by the metalens and that accumulated by the free space propagation, should be a constant. Thus, one could have the following relation:

,          (1)

where x and y are the coordinates of each unit,is the refractive index of the medium,is the design wavelength, f is the focal length,is the incident angle,is the phase at the centre, andis the relative phase of a unit with respect to the centre.

As the metalens is optimized forand the medium is air (), the phase profile could be derived as following assuming=0:

.                   (2)

Fig. S1.  Schematic of the off-axis reflection.

S2.  Parameter optimization

In order to optimize the parameters of our metalens to meet the requirements of AR display, we explored the influence of the height, length and width of the nanorods on both reflection and transmission. To reduce the simulation time, sweeping simulations are conducted in FDTD based on a meta-grating-cell with six gray levels (Fig. S2).

According to the generalized Snell’s law of reflection [1]:

,                           (3)

whereandare the angles of reflection and incidence respectively, is the vacuum wavelength, is the refractive index of the media, andis the constant gradient of phase discontinuity, which is set to berad/nm in our meta-grating-cell, the 1-order diffraction angle is calculated to befor the case of.

We simulated the 1st order diffraction efficiency of the reflected light with the height, length and width of the nanorods varying from 150 nm to 250 nm, from 50 nm to 250 nm, and from 60 nm to 150 nm, respectively, and selected several groups of representative nanorod structures in the region with high diffraction efficiency, to simulate the transmission spectra for normal incident light covering from 400 nm to 700 nm (Fig. S3). Fig. S3, A to F, shows the simulation results of reflection and transmission when fixing the height of the nanorods to be 150 nm, 170 nm, 190 nm, 200 nm, 230 nm and 250 nm, respectively. For each height, we selected three groups of structures with high 1st order diffraction efficiency in reflection (left) and further investigated their transmission characteristics (right). When taking into consideration both the reflection and transmission performances, as well as the availability of samples, we decided to choose the structure with L=160 nm, W=100 nm and H=230 nm, whose characterizes are shown in Fig. S3E (black solid line). Such a structure achieves good transmission performance, with high overall transmittance, and relatively narrow-band troughs, which ensures the transmitted natural light to suffer from little chromatic aberration or distortion. Meanwhile, it achieves a reasonably high diffraction efficiency in reflection ~16.10%. Here, for AR application, since the natural light coming from the real-world scene could not be conveniently manipulated, while the brightness of the virtual images could be artificially adjusted, the characteristics of transmission are weighed slightly heavier than diffraction efficiency of reflection.

Fig. S2.  Six-gray-level meta-grating-cell for simulation. The rotation angles of the nanorods range from 0 degrees to 150 degrees with a step of 30 degrees. (A) Top-view and (B) stereo-view of the meta-grating-cell.

Fig. S3.  Parameter optimization. The 1st order diffraction efficiencies of the reflected light (left), as the length and width of the nanorods vary while the height is fixed to be (A) 150 nm, (B) 170 nm, (C) 190 nm, (D) 200 nm, (E) 230 nm and (F) 250nm, respectively, and the 0th order transmission spectra (right) of the meta-grating-cell, with the corresponding length × width of each nanorod and the 1st diffraction efficiency labeled in the legends.

S3.  Parameter definition

As shown in Fig. S4, a and f denote the aperture size (the diagonal of the square aperture) and the focal length of the metalens respectively, which are fixed after design and fabrication. The numerical aperture (NA) of the metalens is presented as:

,                            (4)

where n denotes the refractive index of the medium.

According to the Maxwellian View display, the collimated image light is reflected and focused to the focal point where the eye pupil is centered. Therefore, the diagonal field of view (FOV) of the AR display is presented as:

.                             (5)

From Eq. (4) and Eq. (5), it can be derived that:

.                              (6)

Fig. S4.  Schematic for critical parameters in the AR near-eye display system based on the reflective metalens.

S4.  Focusing experiments

We conducted focusing experiments based on the optical setup shown in Fig. S5, using a 10 X objective (Olympus UPlanFL N) and a matching tubelens (Thorlabs TTL180-A) to magnify the focal spots. The incident light was set to be right-handed circularly polarized after passing through a right-handed circular polarizer, and the incident angle was precisely adjusted to 45o. In the reflection mode, the incident light is set to be right-handed circularly polarized collimated light at 45o incident angle and wavelength 633 nm. The structure parameters are set as described in the main text. The rotation angle of each nanorod at coordinate (x, y) conforms to Eq. (1) of the main text with λd =633 nm. To compare the experimental results with simulation, we simulated the optical properties of a proportionally downsized metalens, due to the limitation of our computational resources. It possesses a decreased area 7.5×7.5 μm2 (30×30 units) and a shortened focal length 150 μm. Thus, it has the same NA and provides almost equivalent characteristics as the fabricated one. Fig. S6B shows the simulated intensity profile of the metalens at the focal plane (z=150 μm), and Fig. S6C shows the corresponding normalized intensity profiles along the dashed lines in Fig. S6A and S6B. One can see that the measured full width at half maximum (FWHM) 11.49 μm is quite close to the simulated value of 11.34 μm.

Fig. S5.  Optical setup for focusing experiments.

Fig. S6.  Focal spots of the fabricated metalens at the illumination wavelength of 633nm. The area of the simulated metalens is 7.5×7.5 μm2 (30×30 units), and the focal length is 150 μm, while the actual fabricated sample for experiment has an area of 1×1 mm2 (4000×4000 units) and a focal length of 20 mm. (A) Measured intensity profile of the fabricated metalens at the focal plane (z=20 mm). Scale bar, 20 μm. (B) Simulated intensity profile of the metalens at the focal plane (z=150 μm). (C) Corresponding normalized intensity profiles along the dashed lines in (A) and (B) respectively. The FWHM is 11.34 μm for simulation and 11.49 μm for experiment.

S5.  Monochromatic imaging experiments

We first used a black receiving screen to receive the image generated by the metalens at different depths, and Fig. S7 shows the experimental setup. Fig. S8 shows the corresponding imaging results by changing the focus depth of the camera. As seen in Fig. S8A, the dial is visually clear when the camera is right focused at the depth of its position (130 mm). And the camera is focused at the puppet (260 mm) and the rod labeled “R” (400 mm) in Fig. S8, B and C, respectively. It is obvious that the virtual image (“R”) is always clear at any depth.

Then we used a receiving screen with graduated scale to measure the size of images at different depths. Fig. S9A shows the minimum image size right at the focal length of our metalens (almost a point), while Fig. S9, B to D, shows the image sizes at the depths of 92 mm, 170 mm and 250 mm are about 3×3 mm2, 6×6 mm2 and 9×9 mm2, respectively. The further away from the metalens, the bigger the image size is, which confirms the principle of Maxwellian View display.

Fig. S7.  Optical setup for imaging experiments using a receiving screen.

Fig. S8.  Imaging results of the metalens using the receiving screen. The imaging depths (distances between the receiving screen and the metalens) are (A) 130 mm (dial), (B) 260 mm (puppet) and (C) 400 mm (rod labeled “R”), respectively. The virtual images are legible at all depths.

Fig. S9.  Sizes of images on the receiving screen. The distances between the receiving screen and the metalens are (A) 20 mm, (B) 92 mm, (C) 170 mm and (D) 250 mm.

S6.  Maxwellian-view display

The Maxwellian-view display provides a simple way to avoid the vergence-accommodation conflict [2, 3]. The diagram of a typical Maxwellian-view display system is shown in Fig. S10. The light coming from the point source is collimated into parallel light by a condenser and then illuminates the spatial light modulator (SLM). The light modulated by the SLM is subsequently concentrated at the pupil, forming an extremely small exist pupil. In such a system, because each field of the SLM is imaged through a narrow aperture on the pupil (pinhole), clear images would always be formed on the retina regardless of the diopter of the eye lens. Hence, this method can achieve a large depth of field without providing the accommodation depth cue.

Fig. S10.  Schematic of the Maxwellian-view display.

S7.  Eyebox enlargement techniques

The system employing Maxwellian View display technique can effectively resolve the accommodation-convergence conflict, but suffers from having a small eyebox, which makes the virtual image easily missed out as the eye moves. A possible solution to this problem is to utilize multi-view display techniques [4]. As shown in Fig. S11A, the metasurface is divided into multiple areas a1, a2 and a3, and the reflected light from different areas will converge to different viewpoints. Therefore, the human eye can receive parallax images through these viewpoints simultaneously, which can not only provide correct depth cues for the single eye, but also enlarge the exit pupil. Fig. S11B shows another feasible solution to address this problem, which is to adopt pupil duplication technique by multiplexing several holograms on the metasurface [5]. As the metasurface generates multiple focal points at different locations, the human eye can always receive the virtual image when the eye moves laterally within a certain range, which also enlarges the eyebox.

Fig. S11.  Eyebox enlargement techniques. (A) Multiple viewpoints and (B) pupil duplication to enlarge the eyebox.

S8.  Optical setup for color imaging

Fig. S12.  Optical setup for “RGB” imaging experiment with an ideal achromatic metalens.

Fig. S13.  Optical setup for “RGB” imaging experiment with the fabricated metalens. The incident angles of RGB wavelengths are about 0°, 6.48° and 11.34°, respectively.

References

1.	Yu N, Genevet P, Kats MA, Aieta F, Tetienne J-P, Capasso F, et al. Light propagation with phase discontinuities: generalized laws of reflection and refraction. Science. 2011;334:333-7.

2.	Hua H. Enabling focus cues in head-mounted displays. Proc IEEE. 2017;105:805-24.

3.	Takaki Y, Fujimoto N. Flexible retinal image formation by holographic Maxwellian-view display. Opt Express. 2018;26:22985-99.

4.	Jang C, Bang K, Moon S, Kim J, Lee S, Lee B. Retinal 3D: augmented reality near-eye display via pupil-tracked light field projection on retina. ACM Trans Graph. 2017;36:190.

5.	Kim S-B, Park J-H. Optical see-through Maxwellian near-to-eye display with an enlarged eyebox. Opt Lett. 2018;43:767-70.