Table 1 Index properties of Solani river sand

| Properties | Values |
| --- | --- |
| Type | Poorly graded |
| Sand% | 99.42 |
| Silt% | 0.58 |
| Clay% | 0 |
| D10 | 0.151 |
| D30 | 0.219 |
| D60 | 0.315 |
| Coefficient of Uniformity(Cu) | 2.082 |
| Coefficient of curvature(Cc) | 1.018 |
| Specific Gravity(G) | 2.631 |
| Minimum dry density(kg/m3) | 1421 |
| Maximum dry density(kg/m3) | 1604 |
| Coefficient of permeability(m/s) | 9.574×10-5 |
| IS classification | SP |
| Maximum void ratio (emax) Minimum void ratio (emin) | 0.852 0.640 |

Table 2 Properties of PU Foam material

| Material state | Properties | Specification |
| --- | --- | --- |
| Liquid PU Foam | Mix ratio | 1:1 |
|  | Density (kN/m3) | 11 |
|  | Viscosity(Ns/m2) | 0.5 |
|  | Volume expansion factor | 30 |
|  | Time for Hardening (in minutes) | 20 |
|  | Toxicity | Non-toxic |
| Hardened PU Foam (or) Cured PU Foam | Density (kN/m3) | 0.25 |
|  | Bio Degradability | Inert and Non Bio Degradable |
|  | Chemical Resistance | Resistant to organic solvents, mild acids and alkalis |
|  | Energy dissipation | Stiff, light weight, Highly resilient, vibration absorbent and dampener |

Table 3 Experimental schedule adopted for assessing the performance of barrier system

| Schedule Number | Reinforcement type | Relative Density | Day-1 | Day-2 | Day-3 | Day-4 | Day-5 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Unreinforced | 40% | Model ground preparation | 0.1g | 0.2g | 0.3g | 0.4g |
| 2 | Skirted ground reinforcement | 40% | Model ground preparation | 0.1g | 0.2g | 0.3g | 0.4g |
| 3 | Unreinforced | 60% | Model ground preparation | 0.1g | 0.2g | 0.3g | 0.4g |
| 4 | Skirted ground reinforcement | 60% | Model ground preparation | 0.1g | 0.2g | 0.3g | 0.4g |