An aptamer SERS/RRS/Abs trimode biosensor for trace Pb2+ based-liquid crystal@nanosilver catalytic amplification

Yiyi Shu, ShaLi, Aihui Liang, Zhiliang Jiang*

Key Laboratory of Ecology of Rare and Endangered Species and Environmental Protection (Guangxi Normal University), Ministry of Education, Guangxi Key Laboratory of Environmental Pollution Control Theory and Technology, Guilin 541004, China.

A

B

Figure. S1. Stability of AgNPs and CB@AgNPs

A: The RRS signal of AgNPs and CB@AgNPs varying with time; B: The RRS signal of AgNPs and CB@AgNPs varying with NaCl.

a

g

a

f

a

f

F

E

D

C

a

f

B

A

a

f

Figure.S2. SERS spectra of AgNPs /LC -Fo-AgNO3-Apt-inorganic pollutants system

A: AptPb+NaAc-HAc+AgNPs+AgNO3+Fo+VB4r+NaCl, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively. B AptPb+NaAc-HAc+CB+AgNO3+Fo+VB4r+NaCl, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively. C: AptPb+NaAc-HAc+OA+AgNO3+Fo+VB4r+NaCl, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively. D: AptPb+NaAc-HAc+HA+AgNO3+Fo+VB4r+NaCl, a to g represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2, 0.133 and 0.201 nmol/L Pb2+ respectively. E: AptPb+NaAc-HAc+DB+AgNO3+Fo+VB4r+NaCl, a to f represent 0, 4.47×10-3, 6.7×10-3, 6.7×10-2, 0.133 and 0.201 nmol/L Pb2+ respectively. F: AptPb+NaAc-HAc+DE+AgNO3+Fo+VB4r+NaCl, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively.

aa

gg

E

F

D

a

f

a

g

C

a

f

a

g

B

A

a

f

Figure.S3. RRS spectra of AgNPs/LC-Fo-AgNO3-Apt- inorganic pollutants system RRS spectrum system

A: AptPb+NaAc-HAc+AgNPs+AgNO3+Fo, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively. B: AptPb+NaAc-HAc+CB+AgNO3+Fo, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively. C: AptPb+NaAc-HAc+OA+AgNO3+Fo, a to g represent 0, 6.7×10-3, 8.94×10-3, 6.7×10-2, 0.133, 0.201 and 0.267 nmol/L Pb2+ respectively. D: AptPb+NaAc-HAc+HA+AgNO3+Fo, a to g represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133, 0.201 nmol/L Pb2+ respectively. E: AptPb+NaAc-HAc+DB+AgNO3+Fo, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively. F: AptPb+NaAc-HAc+DE+AgNO3+Fo, a to g represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2, 0.133and 0.201 nmol/L Pb2+ respectively.

A

D

B

a

f

a

f

a

f

a

g

Figure. S4. Abs spectra of AptPb AgNPs/LC-Fo-AgNO3-Pb2+ system

A: AptPb+NaAc-HAc+OA+AgNO3+Fo, a to g represent 0, 6.7×10-3, 8.94×10-3, 6.7×10-2, 0.133, 0.201 and 0.267 nmol/L Pb2+ respectively. B: AptPb+NaAc-HAc+HA+AgNO3+Fo, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+respectively. C: AptPb+NaAc-HAc+DB+AgNO3+Fo, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2 and 0.133 nmol/L Pb2+ respectively. DF: AptPb+NaAc-HAc+DE+AgNO3+Fo, a to f represent 0, 4.47×10-3, 6.7×10-3, 8.94×10-3, 6.7×10-2, 0.133nmol/L Pb2+ respectively.

D

A

I

H

G

F

E

B

C

J

Figure. S5. Optimization of analysis conditions

A: AptPb; B: NaAc-HAc; C: AgNO3; D: Fo; E: reaction temperature; F: reaction time; G: CB@AgNPs; H: standing time; I: NaCl; J: VB4r

A

D

F

E

H

G

C

B

Figure. S6. Optimization of RRS analysis conditions

A: AptPb; B: NaAc-HAc; C: AgNO3; D: Fo; E: reaction temperature; F: reaction time; G: CB@AgNPs; H: standing time;

Table S1

Comparison of LC/CB@AgNPs/AgNPs catalytic action and inhibitory action of aptamers

| LC types | Working curve | Linear range | Coefficient(R2) |
| --- | --- | --- | --- |
| CB | △I = 1382.2CCB-62.7 | 0.01-0.1mmol/L | 0.9983 |
| AptPb -CB | △I = 1000.3CApt-13.4 | 0.0667-0.667 nmol/L | 0.9591 |
| OA | △I = 2895.6COA-560.1 | 0.001-0.01 mmol/L | 0.91579 |
| AptPb -OA | △I = 1282.7CApt-486.2 | 0.0667-0.667 nmol/L | 0.90515 |
| HA | △I =2245.5CHA-251.8 | 0.001-0.01 mmol/L | 0.9383 |
| AptPb -HA | △I =3844.5CApt-25.1 | 0.0667-0.667 nmol/L | 0.9334 |
| DB | △I=1072.6CDB- 219.5 | 0.001-0.01 mmol/L | 0.90667 |
| AptPb -DB | △I=1640.7CApt- 1193.9 | 0.0667-0.667 nmol/L | 0.9132 |
| DE | △I= 748.4CDE- 223.2 | 0.001-0.01 mmol/L | 0.9223 |
| AptPb -DE | △I= 1142.7CApt- 594.6 | 0.0667-0.667 nmol/L | 0.9168 |
| CB@AgNPs | △I = 9776.2CCB@AgNPs +5.4 | 0.01-0.133 mmol/L | 0.9991 |
| AptPb - CB@AgNPs | △I= 7983CApt- 278.4 | 0.0667-0.667 nmol/L | 0.9868 |
| AgNPs | △I = 5397.5CAgNPs +1.7 | 0.01-0.133 mmol/L | 0.9963 |
| AptPb -AgNPs | △I= 4378CApt- 304.6 | 0.0667-0.667 nmol/L | 0.9831 |

Table S2

Analysis characteristics of Pb2+ detection by SERS/RRS/Abs

| LCs | Method | Linear range (nmol/L) | Working curve | Coefficient | LD (nmol/L) |
| --- | --- | --- | --- | --- | --- |
| CB@AgNPs | SERS | 4.47×10-3-0.201 | ΔI1618cm-1= 76201C- 414.6 | 0.998 | 3×10-3 |
|  | RRS | 4.47×10-3-0.201 | ΔI370nm= 33687C+ 166 | 0.996 | 3×10-3 |
|  | Abs | 4.47×10-2-0.133 | ΔA430nm= 4.7887C+0.001 | 0.9947 | 2×10-2 |
| AgNPs | SERS | 4.47×10-3-0.133 | ΔI1618cm-1= 55856C+627 | 0.9879 | 3×10-3 |
|  | RRS | 4.47×10-3-0.133 | ΔI370nm= 28594C+ 156 | 0.9929 | 3×10-3 |
|  | Abs | 4.47×10-2-0.133 | ΔA430nm= 3.9979C+0.05 | 0.986 | 2×10-2 |
| CB | SERS | 4.47×10-3-0.133 | ΔI1618cm-1= 14840C- 13.2 | 0.9947 | 3×10-3 |
|  | RRS | 8.94×10-3-0.133 | ΔI370nm= 23444C+ 151.5 | 0.9915 | 5×10-3 |
|  | Abs | 4.47×10-2-0.133 | ΔA430nm= 3.9143C+0.03 | 0.9808 | 2×10-2 |
| OA | SERS | 8.94×10-3-0.133 | ΔI1618cm-1= 9658.8C-8.2 | 0.9888 | 5×10-3 |
|  | RRS | 8.94×10-3-0.267 | ΔI370nm=6444.9C+ 52.7 | 0.9887 | 5×10-3 |
|  | Abs | 6.7×10-2-0.267 | ΔA450nm= 1.7109C+ 0.03 | 0.9687 | 3×10-2 |
| HA | SERS | 8.94×10-3-0.201 | ΔI1618cm-1= 6255.2C+ 8.4 | 0.9887 | 5×10-3 |
|  | RRS | 8.94×10-3-0.201 | ΔI370nm=15079C+ 207.7 | 0.9864 | 5×10-3 |
|  | Abs | 4.47×10-2-0.133 | ΔA450nm= 2.10C+ 0.02 | 0.9457 | 2×10-2 |
| DB | SERS | 8.94×10-3-0.201 | ΔI1618cm-1= 12459C+39.1 | 0.988 | 4×10-3 |
|  | RRS | 8.94×10-3-0.133 | ΔI370nm=22772C+104 | 0.9852 | 5×10-3 |
|  | Abs | 4.47×10-2-0.133 | ΔA440nm=1.0C+ 0.009 | 0.9273 | 2×10-2 |
| DE | SERS | 8.94×10-3-0.133 | ΔI1618cm-1= 7084.9C-14.7 | 0.987 | 5×10-3 |
|  | RRS | 8.94×10-3-0.201 | ΔI370nm=25518C+311.9 | 0.984 | 6×10-3 |
|  | Abs | 6.7×10-2-0.133 | ΔA440nm=3.20C+ 0.05 | 0.917 | 3×10-2 |

Table S3 The analysis characteristics of inorganic pollutants by Apt-CB@AgNPs catalytic SERS/RRS

| Analytes | Method | Linear range (nmol/L) | Working curve | Coefficient | LD (nmol/L) |
| --- | --- | --- | --- | --- | --- |
| Pb2+ | SERS | 4.47×10-3-0.201 | ΔI1618cm-1= 76201C- 414.6 | 0.998 | 3×10-3 |
|  | RRS | 4.47×10-3-0.201 | ΔI370nm= 33687C+ 166 | 0.996 | 3×10-3 |
| As3+ | SERS | 6.67×10-3-0.133 | ΔI1618cm-1= 51005C-92.4 | 0.9877 | 3×10-3 |
|  | RRS | 6.67×10-3-0.133 | ΔI370nm=29280C+ 40.2 | 0.9884 | 3×10-3 |
| Cd2+ | SERS | 6.67×10-3-0.133 | ΔI1618cm-1= 60283C-187.5 | 0.9811 | 3×10-3 |
|  | RRS | 6.67×10-3-0.133 | ΔI370nm=32880C+ 132.7 | 0.9874 | 3×10-3 |
| Hg2+ | SERS | 0.67-30 | ΔI1618cm-1= 228.28C+ 197.8 | 0.9807 | 3 |
|  | RRS | 0.67-30 | ΔI370nm=211.19C+ 343.3 | 0.9867 | 3 |

Table S4

Comparison of analysis characteristics between this method and the reported method

| Method* | Method principle | Linear range /（nmol/L） | DL/（nmol/L） | Annotation | Ref. |
| --- | --- | --- | --- | --- | --- |
| FL | The functional groups on the surface of fluorescent nanoparticles combined with Pb2+ to enhance FL. | 5 - 50 | 3 | The stability is good but the detection range is not wide. | [35] |
| PE | Pb2+ bind to the captured DNA in the detection electrode to cause signal changes. | 0.5 - 900 | 0.166 | High sensitivity but cumbersome substrate synthesis. | [36] |
| FL | The combination of Pb2+ with the AuNP-DNA probe in the detection electrode caused a signal change. | 0 -50 | 2.5 | Good selectivity but complicated electrode modification. | [37] |
| SERS | When Pb2+ bind to ARS, colloidal clusters with high SERS activity were generated, resulting in enhanced Raman signal. | 8 - 20000 | 6 | Fast and convenient but low detection sensitivity. | [38] |
| SERS | Pb(II) and Apt specifically bint to form a G-tetrad structure, and the combination of Pb(II)-Apt tetrad structure and CDAu produced a strong Raman effect. | 1.7 – 13.3 | 0.8 | The selectivity is good, but the operation is more complicated. | [39] |
| Abs | TpPapd-Apt-Pb2+ was combined with the DNA reaction of heme (HM), and there was a surface plasmon resonance (SPR) absorption peak at 395nm. An analytical method for the determination of lead ions had been established. | 0.001 – 0.1 | 0.004 | High sensitivity, fast speed and good selectivity, but the operation is more complicated. | [25] |
| ECL | Pb2+ was captured by Apt 1-PtNPs and formed a G-quadruplex, and then made PtNPs close enough to CdTe QD to cause ECL intensity changes. | 0.1 – 1000 | 0.037 | The detection range is high, but the stability is poor. | [40] |
| SERS | The Apt combined with Pb2+ to form a complex, detached from the surface of CB@AgNPs, and restored its catalysis, which enhanced the SERS signal | 0.0047 – 0.201 | 0.0036 | Sensitive, simple and fast. | This assay |

* FL-fluorescence, PE- photoelectrochemical, ECL-electrochemiluminescence.

Table S5

The influence of interfering ions on the system

| Interfering ion | Relative multiple | Relative error (%) | Interfering ion | Relative multiple | Relative error (%) |
| --- | --- | --- | --- | --- | --- |
| Mg2+ | 1000 | 2.4 | Ca2+ | 1000 | 2.9 |
| Fe3+ | 100 | -1.9 | Zn2+ | 500 | -2.8 |
| Cu2+ | 100 | -6.3 | Al3+ | 500 | -7.1 |
| Co2+ | 500 | -1.4 | Hg2+ | 100 | 3.0 |
| Ba2+ | 1000 | -5.9 | NH4+ | 500 | 1.3 |
| Fe2+ | 1000 | 3.4 | Mn2+ | 1000 | 4.5 |
| Cr6+ | 1000 | 2.1 | Cr3+ | 1000 | -3.1 |
| NO2- | 100 | -1.4 | PO43- | 100 | -5.5 |
| serum protein - | 500 | -2.7 | HSA | 100 | -1.5 |
| BSA- | 1000 | 3.6 | ascorbic acid | 500 | 1.9 |

Table S6

SERS measurement results of the samples

| Sample | Average（nmol/L） | Added Pb2+（nmol/L） | Found（nmol/L） | Recovery (%) | RSD（%） | Content (nmol/L or ng/g) |
| --- | --- | --- | --- | --- | --- | --- |
| Water 1 | 0.1934 | 0.067 | 0.2565 | 94.18 | 5.4 | 0.1945 |
| Water 2 | 0.1801 | 0.067 | 0.2534 | 109.4 | 7.1 | 0.1815 |
| Water 3 | 0.1843 | 0.067 | 0.2556 | 107.8 | 4.3 | 0.1857 |
| Water 4 | 0.3295 | 0.067 | 0.3989 | 103.6 | 6.1 | 0.3310 |
| Preserved eggs 1 | 0.4287 | 0.067 | 0.4995 | 105.67 | 1.3 | 14.796 |
| Preserved eggs 2 | 0.4659 | 0.067 | 0.5298 | 95.37 | 2.9 | 15.173 |
| Preserved eggs 3 | 0.4778 | 0.067 | 0.5482 | 105.07 | 3.5 | 15.389 |
| Preserved eggs 4 | 0.5003 | 0.067 | 0.5623 | 92.53 | 2.5 | 16.653 |
| Orange peel 1 | 0.1003 | 0.067 | 0.1632 | 93.88 | 3.2 | 4.986 |
| Orange peel 2 | 0.1196 | 0.067 | 0.1856 | 98.51 | 6.4 | 5.352 |
| Orange peel 3 | 0.1284 | 0.067 | 0.1987 | 104.9 | 5.1 | 5.435 |
| Orange peel 4 | 0.1467 | 0.067 | 0.2156 | 102.8 | 2.9 | 5.683 |