Supporting information – ZnO NRs

Figure S1 (a) Cross-section SE image at 10 kV of as-grown ZnO NRs at 90°C for 3 hours on a drop-casted seeded substrate. The scale bar represents 200 nm. (b) Top-view SE image at 10 kV of the same sample, showing very good coverage of ZnO NRs over a large area of substrate. The scale bar denotes 2 µm.

Exemplary, Figure S1 (a) shows a 10 kV-SE image at of a typical cross-section of a ZnO NR film grown at 90°C for 3 hours on a drop-casted seeded substrate. To demonstrate the very good coverage of the ZnO NRs over the seeded substrate, a low magnification top-view SE image of the same sample as in Figure S1 (a) is shown in Figure S1 (b). The precise calculation of the density of NRs (per µm2) was not possible due to the large angular distribution of the NRs with respect to the substrate normal.

Fig. S2 shows the low temperature CL spectra of the a-plane ZnO single crystal with varying acceleration voltage from 5 kV to 15 kV. A 2-fold enhancement of the UV emission can be observed at HV = 5 kV which can be translated to a probing depth (70% electron energy loss) of 100 nm for the Au NP-coated half of the sample. At higher HV (probing depth of approximately 350 nm for 10 kV and 550 nm for 15 kV), a decreased enhancement of approximately 1.4 is found, agreeing with the Au-ZnO interaction being strongest close to the surface (cf. Table 4 in main text).

Figure S2 CL spectra of uncoated (solid) and Au NP-coated (dotted) a-plane ZnO single crystal at T = 10 K and varying the acceleration voltage from 5 to 15 kV.