Supporting Information

for

Ambient Environment Adaptive Elastomer Constructed by Microphase Separation and Segment Complexation of Triblock Copolymers

Weijie Wang, Caihong Zhang, Hao Huang, Bing Xue, Shuguang Yang *

State Key Laboratory for Modification of Chemical Fibers and Polymer Materials, Center for Advanced Low-dimension Materials, College of Materials Science and Engineering, Donghua University, Shanghai 201620, P. R. China

*To whom correspondence should be addressed: shgyang@dhu.edu.cn

Table of Contents

1. Supporting Video

Video S1 Drawing of SAS/SES (A3E) complex.

Video S2 Swing of SAS/SES (A3E) strip when the finger approached.

2. Experiment Section

Material

Synthesis process

Scheme S1 Synthesis route for SAS and SES triblock copolymers.

Characterization

Table S1 Molecular information of SAS and SES triblock copolymers.

3. Supporting Figures

Figure S1 GPC evolution curves of the different molecular weight PS-PtBA-PS triblock copolymers.

Figure S2 FT-IR spectra of triblock copolymer PS-PtBA-PS and SAS triblock copolymers.

Figure S3 1H NMR spectra of SAS.

Figure S4 GPC evolution curve of SES.

Figure S5 SAXS curves of triblock copolymers a) SES and b) SAS.

Figure S6 a) Stress-strain curves and b) IR spectra of SAS/SES complexes before and after alkaline solution (pH 13) treatment.

Figure S7 TGA curves of SAS/SES complex (A3E) incubated with different humidity at 25 ℃.

Figure S8 Damping capacity in each cycle as a function of strain at relative humidity RH 25%, RH 55%, and RH 90% conditions.

2. Experimental Section

Materials. N3-PEO40k-N3 was purchased from Sinopeg Chemical Reagent Co. with the molecular weight Mn = 40 000 and PDI = 1.01. 3-Butyn-1-ol (98%), 4-dimethylaminopyridine (DMAP, 98%), N,N′-diisopropylcarbodiimide (DIPC, 98%), N,N,N′,N″,N″-pentamethyl diethylenetriamine (PMDETA, 95%) were purchased from Adamas and used as received. Trifluoroacetic acid (TFA, 98%), 1,4-dioxane (99%), were purchased from Greagent and used with no further purification. Toluene and dichloromethane (DCM) were treated by solvent purification system. CuBr (98%, Maklin) was washed with acetic acid and acetone, filtered and stored under nitrogen atmosphere. 2,2'-Azobis(2-methylpropionitrile) (AIBN, 98%, Macklin) was recrystallized with ethanol. Styrene (99%, Aladdin) and tert-butyl acrylate (98%, Macklin) were purified by passing a basic alumina column. S-1-Dodecyl-S'-(,'-dimethyl-''-acetic acid) trithiocarbonate (RAFT-COOH) and S,S'-bis(,'-dimethyl-''-acetic acid)-trithioccarbonate (HOOC-RAFT-COOH) were prepared referring the reported reference.[1]

Synthesis process

Triblock copolymers polystyrene-b-poly(acrylic acid)-b-polystyrene (SAS) and polystyrene-b-poly(ethylene oxide)-b-polystyrene (SES) were synthesized apply reversible addition fragmentation chain transfer (RAFT) polymerization. The synthesis routes for SAS and SES are shown in Scheme S1. SAS triblock copolymers were prepared by hydrolysis of the PS-PtBA-PS triblock copolymers. The PS-PtBA-PS triblock copolymers were synthesized by two steps RAFT polymerization. First, by RAFT polymerizing styrene to obtain the macromolecular RAFT agent PS-RAFT-PS. Then polymerizing tert-butyl acrylate to obtain PS-PtBA-PS triblock copolymer. SES triblock copolymer was prepared by first synthesis the RAFT-PEO-RAFT macromolecular RAFT agent by “click chemistry”, then obtained the target SES by polymerizing styrene.

Scheme S1 Synthesis route for SAS and SES triblock copolymers.

Characterization.

1H Nuclear Magnetic Resonance (1H NMR) spectra were acquired using DMSO and DMF as co-solvent (99% D, J&K Chemicals) with a Bruker 600 MHz NMR spectrometer. The 1H NMR spectra were referenced to the residual proton impurities in DMSO at δ 2.5 ppm.

Gel Permeation Chromatography (GPC) was performed using Waters Instrument (515/2410/2487) with THF as the eluent at a flow rate of 1.0 mL min-1 at 40 ℃ and using polystyrenes as standards.

Fourier Transform Infrared (FT-IR) spectra were recorded on a Bruker spectrometer (Vertex 70) with a Single-Bounce ATR attachment.

The results of the synthesis

The structure of target triblock copolymers SAS was confirmed by GPC, FT-IR, and 1H NMR (Figure S1-S3). The GPC evolution curves are monodispersed, indicating the correct of PS-PtBA-PS triblock. In the FT-IR spectra, the C=O absorbance peak shifted from 1721 cm-1 to 1697 cm-1, and the tert-butyl groups disappeared at 1365 cm-1. In addition, in 1H NMR spectra, the peak of the tert-butyl groups at around 1.40 ppm disappeared. The IR and NMR result illustrate the tert-butyl groups are hydrolyzed. GPC curve of SES triblock copolymer shows a monodisperse peak (Figure S4), meaning the accuracy of SES triblock. The molecular information of SAS and SES triblock copolymers is shown in Table S1.

Table S1 Molecular information of SAS and SES triblock copolymers.

| No. | Block information | PDI | PS fraction (wt.%) |
| --- | --- | --- | --- |
| A1 | S10kA28kS10k | 1.49 | 42 |
| A2 | S10kA52kS10k | 1.60 | 28 |
| A3 | S10kA65kS10k | 1.57 | 24 |
| A4 | S10kA120kS10k | 1.61 | 14 |
| E | S15kE40kS15k | 1.09 | 43 |

3. Supporting Figures

Figure S1 GPC evolution curves of the different molecular weight PS-PtBA-PS triblock copolymers.

Figure S2 FT-IR spectra of triblock copolymer PS-PtBA-PS and SAS triblock copolymers.

Figure S3 1H NMR spectra of SAS.

Figure S4 GPC evolution curve of SES.

Figure S5 SAXS curves of triblock copolymers a) SES and b) SAS.

Figure S6 a) Stress-strain curves and b) IR spectra of SAS/SES complex (A3E) before and after alkaline solution (pH 13) treatment.

Figure S7 TGA curves of SAS/SES complex (A3E) incubated with different humidity at 25 ℃.

Figure S8 Damping capacity in each cycle as a function of strain at relative humidity RH 25%, RH 55%, and RH 90% conditions, which indicates the ability to absorb energy of elastomer A3E.

Reference

[1] J. T. Lai, D. Filla, R. Shea, Macromolecules 2002, 35, 6754.