Supporting information

Electrospun Polyacrylonitrile/cellulose nanofibers supported gold nanoparticles for liquid-phase aerobic oxidation of benzyl alcohol to benzaldehyde

Table of Contents

Fig. S1. SEM images and diameter distributions of the PC nanofibers (a) PC_0-1; (b) PC_1-3; (c) PC_1-1; (d) PC_3-1; (e) PC_0-1 at voltage of 20kV.

Fig. S2. TGA and Heat flow profiles under oxygen (red line) and nitrogen (black line) atmosphere of the PC_31 nanofibers.

Fig. S3. Conversion of BzOH obtained with the different AuNPs-nanofibers.

Fig. S4. AuNPs/PC_31

Fig. S4. Dependence of BzOH conversion on the reaction time over AuNPs/PC_31 with and without filtration of the catalyst.

Table S1. BET measurement results of different samples

Fig. S1. SEM images and diameter distributions of the PC nanofibers (a) PC_0-1; (b) PC_1-3; (c) PC_1-1; (d) PC_3-1; (e) PC_0-1 at voltage of 20kV.

Fig. S2. TGA and Heat flow profiles under oxygen (red line) and nitrogen (black line) atmosphere of the PC_31 nanofibers

Fig. S3. Conversion of BzOH obtained with the different AuNPs-nanofibers.

Fig. S4. The photo of the catalyst AuNPs_PC-3-1 (fresh)

Fig. S5. Dependence of BzOH conversion on the reaction time over AuNPs/PC_31 with and without filtration of the catalyst.

Table S1. BET measurement results of different samples

| Catalyst | Surface area (m2/g) |  | Pore width (nm) |
| --- | --- | --- | --- |
| PC-10 | 16.3 | 11.47 |  |
| PC-11 | 37.5 | 17.31 |  |
| PC-31 | 40.1 | 18.15 |  |
| PC-13 | 38.1 | 16.54 |  |
| PC-01 | 52.3 | 22.31 |  |
| AuNPs/PC͢͢-31 | 40.5 | 19.14 |  |