# Supplementary materials

Table S1 Laser oscillation parameters used in the DXR experiments. Note that five simulations were run at the parameters highlighted in bold.

| Case # | Power (W) | Linear speed (mm/s) | Circular oscillation amplitude (mm) | Sample # | Power (W) | Linear speed (mm/s) | Circular oscillation amplitude (mm) | Case # | Power (W) | Linear speed (mm/s) | Circular oscillation amplitude (mm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 300 | 1200 | 0 | 31 | 400 | 1200 | 0 | 61 | 500 | 1200 | 0 |
| 2 | 300 | 1000 | 0 | 32 | 400 | 1000 | 0 | 62 | 500 | 1000 | 0 |
| 3 | 300 | 800 | 0 | 33 | 400 | 800 | 0 | 63 | 500 | 800 | 0 |
| 4 | 300 | 600 | 0 | 34 | 400 | 600 | 0 | 64 | 500 | 600 | 0 |
| 5 | 300 | 400 | 0 | 35 | 400 | 400 | 0 | 65 | 500 | 400 | 0 |
| 6 | 300 | 200 | 0 | 36 | 400 | 200 | 0 | 66 | 500 | 200 | 0 |
| 7 | 300 | 1200 | 0.09 | 37 | 400 | 1200 | 0.09 | 67 | 500 | 1200 | 0.09 |
| 8 | 300 | 1000 | 0.09 | 38 | 400 | 1000 | 0.09 | 68 | 500 | 1000 | 0.09 |
| 9 | 300 | 800 | 0.09 | 39 | 400 | 800 | 0.09 | 69 | 500 | 800 | 0.09 |
| 10 | 300 | 600 | 0.09 | 40 | 400 | 600 | 0.09 | 70 | 500 | 600 | 0.09 |
| 11 | 300 | 400 | 0.09 | 41 | 400 | 400 | 0.09 | 71 | 500 | 400 | 0.09 |
| 12 | 300 | 200 | 0.09 | 42 | 400 | 200 | 0.09 | 72 | 500 | 200 | 0.09 |
| 13 | 300 | 1200 | 0.12 | 43 | 400 | 1200 | 0.12 | 73 | 500 | 1200 | 0.12 |
| 14 | 300 | 1000 | 0.12 | 44 | 400 | 1000 | 0.12 | 74 | 500 | 1000 | 0.12 |
| 15 | 300 | 800 | 0.12 | 45 | 400 | 800 | 0.12 | 75 | 500 | 800 | 0.12 |
| 16 | 300 | 600 | 0.12 | 46 | 400 | 600 | 0.12 | 76 | 500 | 600 | 0.12 |
| 17 | 300 | 400 | 0.12 | 47 | 400 | 400 | 0.12 | 77 | 500 | 400 | 0.12 |
| 18 | 300 | 200 | 0.12 | 48 | 400 | 200 | 0.12 | 78 | 500 | 200 | 0.12 |
| 19 | 300 | 1200 | 0.18 | 49 | 400 | 1200 | 0.18 | 79 | 500 | 1200 | 0.18 |
| 20 | 300 | 1000 | 0.18 | 50 | 400 | 1000 | 0.18 | 80 | 500 | 1000 | 0.18 |
| 21 | 300 | 800 | 0.18 | 51 | 400 | 800 | 0.18 | 81 | 500 | 800 | 0.18 |
| 22 | 300 | 600 | 0.18 | 52 | 400 | 600 | 0.18 | 82 | 500 | 600 | 0.18 |
| 23 | 300 | 400 | 0.18 | 53 | 400 | 400 | 0.18 | 83 | 500 | 400 | 0.18 |
| 24 | 300 | 200 | 0.18 | 54 | 400 | 200 | 0.18 | 84 | 500 | 200 | 0.18 |
| 25 | 300 | 1200 | 0.24 | 55 | 400 | 1200 | 0.24 | 85 | 500 | 1200 | 0.24 |
| 26 | 300 | 1000 | 0.24 | 56 | 400 | 1000 | 0.24 | 86 | 500 | 1000 | 0.24 |
| 27 | 300 | 800 | 0.24 | 57 | 400 | 800 | 0.24 | 87 | 500 | 800 | 0.24 |
| 28 | 300 | 600 | 0.24 | 58 | 400 | 600 | 0.24 | 88 | 500 | 600 | 0.24 |
| 29 | 300 | 400 | 0.24 | 59 | 400 | 400 | 0.24 | 89 | 500 | 400 | 0.24 |
| 30 | 300 | 200 | 0.24 | 60 | 400 | 200 | 0.24 | 90 | 500 | 200 | 0.24 |