Supplementary information for:
Intrinsic Dense Twinning via Release of Native Strain

Xianqi Song,1,4 Chang Liu,1,2,4 Quan Li,1,2,✉ Yanming Ma,1,2,✉ and Changfeng Chen3,✉

1 State Key Lab of Superhard Materials and International Center for Computational Method and Software, College of Physics, Jilin University, Changchun 130012, China

2 International Center of Future Science, Jilin University, Changchun 130012, China

3 Department of Physics and Astronomy, University of Nevada, Las Vegas, Nevada 89154, USA

4These authors contributed equally: Xianqi Song, Chang Liu

✉Corresponding author:

liquan777@jlu.edu.cn (Q. Li);

mym@jlu.edu.cn (Y. Ma);

changfeng.chen@unlv.edu (C. Chen).

Here we provide additional details supporting selected contents in the main text, including structural information for the 1-, 2-, and 3-layer-thick B4C twinning structures, bond lengths in the icosahedral cages of single crystal and 1-layer-thick B4C twinning structures, and snapshots for twinned B4C in different crystal orientations and for several other boron-rich solids containing icosahedral cages.

Supplementary Figure 1-2

Supplementary Table 1-4

Supplementary Figure 1. The twinned crystals of B4C. The twinned B4C crystals with a (111) and b (101) oriented twin planes marked by the vertical solid lines. The carbon atoms on the CBC chains, on the icosahedra, and the boron atoms are represented by lavender, red, and gray spheres, respectively.

Supplementary Figure 2. Structural snapshot of the single crystal (left) and constructed twinned crystal (right) of selected boron-rich solids containing icosahedral cages. The N (and O, P, S), C, and B atoms are represented by pink, lavender, and gray spheres, respectively. The vertical dashed lines represent the TPs. The red one-way (double) arrows indicate the orientation and symmetry of 3-atom chains or distribution of the X atom in the single crystal and twinned crystal of selected boron-rich solids.

Supplementary Table 1. Calculated lattice constants and atomic coordinates for the 1-layer-thick twinned B4C.

|  | Twin A1 |  |  | Twin S1 |  |  | Twin R1 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Parameter (Å, °) | a = 5.145 | b = 5.145 | c = 8.759 | a = 5.145 | b = 4.992 | c = 8.961 | a = 5.160 | b = 4.987 | c = 8.949 |
|  | α = 90.000 | β = 90.000 | γ = 65.486 | α = 90.000 | β = 90.000 | γ = 66.179 | α = 90.000 | β = 90.000 | γ = 65.960 |
| Atoms | x | y | z | x | y | z | x | y | z |
| B1 | 0.169 | 0.678 | 0.899 | 0.183 | 0.685 | 0.901 | 0.182 | 0.679 | 0.901 |
| B2 | 0.032 | 0.032 | 0.657 | 0.330 | 0.319 | 0.835 | 0.328 | 0.313 | 0.835 |
| B3 | 0.678 | 0.169 | 0.899 | 0.025 | 0.028 | 0.656 | 0.028 | 0.034 | 0.656 |
| B4 | 0.238 | 0.238 | 0.668 | 0.688 | 0.171 | 0.900 | 0.686 | 0.163 | 0.900 |
| B5 | 0.524 | 0.524 | 0.836 | 0.232 | 0.238 | 0.662 | 0.231 | 0.246 | 0.660 |
| B6 | 0.386 | 0.881 | 0.596 | 0.533 | 0.533 | 0.840 | 0.531 | 0.525 | 0.840 |
| B7 | 0.881 | 0.386 | 0.596 | 0.376 | 0.874 | 0.594 | 0.377 | 0.880 | 0.594 |
| B8 | 0.774 | 0.774 | 0.745 | 0.875 | 0.388 | 0.595 | 0.873 | 0.397 | 0.595 |
| B9 | 0.174 | 0.678 | 0.096 | 0.777 | 0.771 | 0.747 | 0.780 | 0.780 | 0.748 |
| B10 | 0.321 | 0.321 | 0.168 | 0.183 | 0.685 | 0.094 | 0.182 | 0.679 | 0.094 |
| B11 | 0.036 | 0.036 | 0.336 | 0.330 | 0.319 | 0.160 | 0.328 | 0.313 | 0.160 |
| B12 | 0.807 | 0.128 | 0.495 | 0.025 | 0.028 | 0.339 | 0.028 | 0.034 | 0.340 |
| B13 | 0.093 | 0.414 | 0.998 | 0.799 | 0.119 | 0.498 | 0.798 | 0.127 | 0.498 |
| B14 | 0.678 | 0.174 | 0.096 | 0.109 | 0.413 | 0.998 | 0.104 | 0.410 | 0.998 |
| B15 | 0.527 | 0.527 | 0.157 | 0.688 | 0.171 | 0.096 | 0.686 | 0.163 | 0.095 |
| B16 | 0.145 | 0.466 | 0.498 | 0.232 | 0.238 | 0.334 | 0.231 | 0.246 | 0.335 |
| B17 | 0.431 | 0.752 | 0.995 | 0.533 | 0.533 | 0.155 | 0.531 | 0.525 | 0.156 |
| B18 | 0.390 | 0.881 | 0.399 | 0.137 | 0.474 | 0.498 | 0.136 | 0.482 | 0.498 |
| B19 | 0.466 | 0.145 | 0.498 | 0.440 | 0.772 | 0.998 | 0.377 | 0.880 | 0.401 |
| B20 | 0.752 | 0.431 | 0.995 | 0.376 | 0.874 | 0.401 | 0.455 | 0.149 | 0.498 |
| B21 | 0.881 | 0.390 | 0.399 | 0.455 | 0.143 | 0.498 | 0.761 | 0.432 | 0.998 |
| B22 | 0.785 | 0.785 | 0.245 | 0.765 | 0.437 | 0.998 | 0.873 | 0.397 | 0.400 |
| B23 | 0.414 | 0.093 | 0.998 | 0.875 | 0.388 | 0.401 | 0.780 | 0.780 | 0.248 |
| B24 | 0.128 | 0.807 | 0.495 | 0.777 | 0.771 | 0.249 | 0.424 | 0.077 | 0.998 |
| C1 | 0.325 | 0.325 | 0.839 | 0.428 | 0.105 | 0.998 | 0.438 | 0.743 | 0.998 |
| C2 | 0.234 | 0.234 | 0.339 | 0.119 | 0.811 | 0.498 | 0.121 | 0.817 | 0.498 |
| C3 | 0.927 | 0.927 | 0.805 | 0.934 | 0.923 | 0.808 | 0.944 | 0.925 | 0.808 |
| C4 | 0.621 | 0.621 | 0.686 | 0.615 | 0.626 | 0.683 | 0.615 | 0.635 | 0.688 |
| C5 | 0.938 | 0.938 | 0.186 | 0.934 | 0.923 | 0.187 | 0.944 | 0.925 | 0.188 |
| C6 | 0.632 | 0.632 | 0.305 | 0.615 | 0.626 | 0.313 | 0.615 | 0.635 | 0.308 |

Supplementary Table 2. Calculated lattice constants and atomic coordinates for the 2-layer-thick twinned B4C.

|  | Twin A2 |  |  | Twin S2 |  |  | Twin R2 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Parameter (Å, °) | a = 5.146 | b = 5.146 | c = 17.510 | a = 5.146 | b = 4.991 | c = 17.920 | a = 5.153 | b = 4.988 | c = 17.908 |
|  | α = 90.000 | β = 90.000 | γ = 65.303 | α = 90.000 | β = 90.000 | γ = 66.148 | α = 90.000 | β = 90.000 | γ = 66.046 |
| Atoms | x | y | z | x | y | z | x | y | z |
| B1 | 0.416 | 0.096 | 0.747 | 0.731 | 0.055 | 0.000 | 0.120 | 0.475 | 0.500 |
| B2 | 0.699 | 0.376 | 0.000 | 0.122 | 0.468 | 0.500 | 0.216 | 0.240 | 0.581 |
| B3 | 0.137 | 0.815 | 0.499 | 0.427 | 0.761 | 0.752 | 0.522 | 0.517 | 0.832 |
| B4 | 0.174 | 0.684 | 0.701 | 0.217 | 0.232 | 0.582 | 0.668 | 0.151 | 0.798 |
| B5 | 0.451 | 0.964 | 0.950 | 0.523 | 0.521 | 0.832 | 0.361 | 0.874 | 0.548 |
| B6 | 0.041 | 0.041 | 0.580 | 0.667 | 0.158 | 0.798 | 0.516 | 0.518 | 0.671 |
| B7 | 0.320 | 0.320 | 0.829 | 0.361 | 0.868 | 0.548 | 0.825 | 0.807 | 0.921 |
| B8 | 0.815 | 0.137 | 0.499 | 0.518 | 0.525 | 0.672 | 0.671 | 0.155 | 0.701 |
| B9 | 0.096 | 0.416 | 0.747 | 0.823 | 0.816 | 0.921 | 0.978 | 0.446 | 0.952 |
| B10 | 0.376 | 0.699 | 0.000 | 0.672 | 0.163 | 0.701 | 0.440 | 0.143 | 0.500 |
| B11 | 0.684 | 0.174 | 0.701 | 0.980 | 0.453 | 0.951 | 0.744 | 0.424 | 0.751 |
| B12 | 0.964 | 0.451 | 0.950 | 0.440 | 0.137 | 0.500 | 0.053 | 0.715 | 0.000 |
| B13 | 0.247 | 0.247 | 0.584 | 0.748 | 0.428 | 0.751 | 0.073 | 0.066 | 0.875 |
| B14 | 0.525 | 0.525 | 0.836 | 0.056 | 0.720 | 0.000 | 0.765 | 0.773 | 0.625 |
| B15 | 0.529 | 0.529 | 0.671 | 0.067 | 0.053 | 0.874 | 0.783 | 0.120 | 0.500 |
| B16 | 0.806 | 0.806 | 0.919 | 0.764 | 0.763 | 0.625 | 0.087 | 0.401 | 0.749 |
| B17 | 0.713 | 0.036 | 0.999 | 0.783 | 0.113 | 0.500 | 0.396 | 0.692 | 1.000 |
| B18 | 0.152 | 0.475 | 0.500 | 0.092 | 0.404 | 0.749 | 0.858 | 0.390 | 0.549 |
| B19 | 0.433 | 0.756 | 0.752 | 0.399 | 0.696 | 0.000 | 0.163 | 0.666 | 0.799 |
| B20 | 0.673 | 0.167 | 0.799 | 0.859 | 0.382 | 0.548 | 0.013 | 0.027 | 0.579 |
| B21 | 0.395 | 0.888 | 0.550 | 0.165 | 0.672 | 0.799 | 0.318 | 0.303 | 0.828 |
| B22 | 0.475 | 0.152 | 0.500 | 0.011 | 0.021 | 0.579 | 0.167 | 0.672 | 0.702 |
| B23 | 0.756 | 0.433 | 0.752 | 0.317 | 0.311 | 0.829 | 0.475 | 0.962 | 0.952 |
| B24 | 0.036 | 0.713 | 0.999 | 0.169 | 0.677 | 0.702 | 0.313 | 0.306 | 0.668 |
| B25 | 0.888 | 0.395 | 0.550 | 0.474 | 0.969 | 0.952 | 0.619 | 0.597 | 0.918 |
| B26 | 0.167 | 0.673 | 0.799 | 0.314 | 0.312 | 0.668 | 0.426 | 0.768 | 0.248 |
| B27 | 0.057 | 0.057 | 0.872 | 0.621 | 0.601 | 0.919 | 0.216 | 0.238 | 0.418 |
| B28 | 0.782 | 0.782 | 0.624 | 0.427 | 0.761 | 0.248 | 0.522 | 0.529 | 0.168 |
| B29 | 0.418 | 0.095 | 0.252 | 0.217 | 0.232 | 0.418 | 0.668 | 0.164 | 0.202 |
| B30 | 0.177 | 0.683 | 0.299 | 0.523 | 0.521 | 0.168 | 0.361 | 0.874 | 0.452 |
| B31 | 0.456 | 0.963 | 0.050 | 0.667 | 0.158 | 0.202 | 0.517 | 0.532 | 0.328 |
| B32 | 0.325 | 0.325 | 0.336 | 0.361 | 0.868 | 0.452 | 0.823 | 0.808 | 0.079 |
| B33 | 0.604 | 0.604 | 0.084 | 0.518 | 0.525 | 0.328 | 0.672 | 0.169 | 0.299 |
| B34 | 0.044 | 0.044 | 0.419 | 0.823 | 0.816 | 0.079 | 0.978 | 0.445 | 0.049 |
| B35 | 0.321 | 0.321 | 0.171 | 0.672 | 0.163 | 0.299 | 0.748 | 0.434 | 0.249 |
| B36 | 0.095 | 0.418 | 0.252 | 0.98 | 0.453 | 0.049 | 0.070 | 0.062 | 0.125 |
| B37 | 0.683 | 0.177 | 0.299 | 0.748 | 0.428 | 0.249 | 0.762 | 0.769 | 0.375 |
| B38 | 0.963 | 0.456 | 0.050 | 0.067 | 0.053 | 0.126 | 0.091 | 0.411 | 0.251 |
| B39 | 0.531 | 0.531 | 0.329 | 0.764 | 0.763 | 0.375 | 0.858 | 0.389 | 0.452 |
| B40 | 0.810 | 0.810 | 0.080 | 0.092 | 0.404 | 0.251 | 0.164 | 0.680 | 0.201 |
| B41 | 0.434 | 0.754 | 0.247 | 0.859 | 0.382 | 0.452 | 0.010 | 0.028 | 0.421 |
| B42 | 0.677 | 0.166 | 0.201 | 0.165 | 0.672 | 0.201 | 0.319 | 0.317 | 0.171 |
| B43 | 0.399 | 0.887 | 0.450 | 0.011 | 0.021 | 0.421 | 0.167 | 0.684 | 0.298 |
| B44 | 0.754 | 0.434 | 0.247 | 0.317 | 0.311 | 0.171 | 0.474 | 0.962 | 0.048 |
| B45 | 0.887 | 0.399 | 0.450 | 0.169 | 0.677 | 0.298 | 0.314 | 0.318 | 0.332 |
| B46 | 0.166 | 0.677 | 0.201 | 0.474 | 0.969 | 0.048 | 0.619 | 0.595 | 0.081 |
| B47 | 0.068 | 0.068 | 0.124 | 0.314 | 0.312 | 0.332 | 0.410 | 0.067 | 0.748 |
| B48 | 0.793 | 0.793 | 0.372 | 0.621 | 0.601 | 0.081 | 0.715 | 0.360 | 1.000 |
| C1 | 0.331 | 0.331 | 0.669 | 0.411 | 0.096 | 0.748 | 0.731 | 0.025 | 0.000 |
| C2 | 0.608 | 0.608 | 0.921 | 0.719 | 0.388 | 0.000 | 0.424 | 0.733 | 0.751 |
| C3 | 0.242 | 0.242 | 0.421 | 0.104 | 0.804 | 0.500 | 0.104 | 0.810 | 0.500 |
| C4 | 0.519 | 0.519 | 0.169 | 0.600 | 0.620 | 0.593 | 0.599 | 0.629 | 0.595 |
| C5 | 0.211 | 0.211 | 0.902 | 0.905 | 0.910 | 0.843 | 0.915 | 0.914 | 0.845 |
| C6 | 0.936 | 0.936 | 0.654 | 0.225 | 0.205 | 0.905 | 0.236 | 0.209 | 0.907 |
| C7 | 0.629 | 0.629 | 0.596 | 0.921 | 0.916 | 0.655 | 0.931 | 0.917 | 0.655 |
| C8 | 0.903 | 0.903 | 0.844 | 0.411 | 0.096 | 0.252 | 0.412 | 0.102 | 0.251 |
| C9 | 0.221 | 0.221 | 0.096 | 0.600 | 0.620 | 0.407 | 0.599 | 0.627 | 0.407 |
| C10 | 0.947 | 0.947 | 0.344 | 0.905 | 0.910 | 0.157 | 0.904 | 0.918 | 0.155 |
| C11 | 0.640 | 0.640 | 0.402 | 0.225 | 0.205 | 0.095 | 0.236 | 0.207 | 0.095 |
| C12 | 0.915 | 0.915 | 0.154 | 0.921 | 0.916 | 0.345 | 0.920 | 0.922 | 0.345 |

Supplementary Table 3. Calculated lattice constants and atomic coordinates for the 3-layer-thick twinned B4C.

|  | Twin A3 |  |  | Twin S3 |  |  | Twin R3 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Parameter (Å, °) | a = 5.147 | b = 5.147 | c = 26.265 | a = 5.146 | b = 4.991 | c = 26.879 | a = 5.151 | b = 4.989 | c = 26.867 |
|  | α = 90.000 | β = 90.000 | γ = 65.248 | α = 90.000 | β = 90.000 | γ = 66.141 | α = 90.000 | β = 90.000 | γ = 66.072 |
| Atoms | x | y | z | x | y | z | x | y | z |
| B1 | 0.698 | 0.021 | 0.999 | 0.739 | 0.054 | 0.000 | 0.821 | 0.185 | 0.500 |
| B2 | 0.860 | 0.183 | 0.500 | 0.822 | 0.178 | 0.500 | 0.222 | 0.228 | 0.721 |
| B3 | 0.141 | 0.465 | 0.668 | 0.128 | 0.471 | 0.668 | 0.529 | 0.516 | 0.888 |
| B4 | 0.417 | 0.741 | 0.835 | 0.435 | 0.760 | 0.835 | 0.917 | 0.950 | 0.554 |
| B5 | 0.234 | 0.234 | 0.724 | 0.224 | 0.232 | 0.722 | 0.675 | 0.150 | 0.865 |
| B6 | 0.510 | 0.510 | 0.891 | 0.531 | 0.521 | 0.888 | 0.062 | 0.583 | 0.532 |
| B7 | 0.955 | 0.955 | 0.556 | 0.918 | 0.942 | 0.555 | 0.369 | 0.861 | 0.698 |
| B8 | 0.659 | 0.152 | 0.866 | 0.675 | 0.157 | 0.865 | 0.833 | 0.806 | 0.947 |
| B9 | 0.103 | 0.596 | 0.533 | 0.062 | 0.577 | 0.532 | 0.217 | 0.228 | 0.614 |
| B10 | 0.383 | 0.875 | 0.700 | 0.369 | 0.867 | 0.699 | 0.527 | 0.517 | 0.781 |
| B11 | 0.791 | 0.791 | 0.946 | 0.831 | 0.815 | 0.948 | 0.985 | 0.445 | 0.968 |
| B12 | 0.238 | 0.238 | 0.614 | 0.219 | 0.235 | 0.615 | 0.372 | 0.865 | 0.634 |
| B13 | 0.514 | 0.514 | 0.781 | 0.525 | 0.525 | 0.781 | 0.679 | 0.155 | 0.801 |
| B14 | 0.948 | 0.436 | 0.967 | 0.988 | 0.453 | 0.967 | 0.445 | 0.134 | 0.667 |
| B15 | 0.393 | 0.882 | 0.634 | 0.373 | 0.873 | 0.634 | 0.752 | 0.424 | 0.834 |
| B16 | 0.670 | 0.158 | 0.800 | 0.681 | 0.162 | 0.800 | 0.060 | 0.714 | 0.000 |
| B17 | 0.465 | 0.141 | 0.668 | 0.449 | 0.138 | 0.667 | 0.141 | 0.853 | 0.500 |
| B18 | 0.741 | 0.417 | 0.835 | 0.756 | 0.427 | 0.834 | 0.081 | 0.064 | 0.917 |
| B19 | 0.021 | 0.698 | 0.999 | 0.064 | 0.719 | 0.000 | 0.466 | 0.482 | 0.584 |
| B20 | 0.183 | 0.860 | 0.500 | 0.141 | 0.846 | 0.500 | 0.775 | 0.775 | 0.750 |
| B21 | 0.042 | 0.042 | 0.915 | 0.075 | 0.053 | 0.916 | 0.788 | 0.111 | 0.666 |
| B22 | 0.491 | 0.491 | 0.583 | 0.464 | 0.473 | 0.583 | 0.096 | 0.400 | 0.833 |
| B23 | 0.767 | 0.767 | 0.749 | 0.770 | 0.763 | 0.750 | 0.484 | 0.830 | 0.500 |
| B24 | 0.805 | 0.125 | 0.665 | 0.793 | 0.114 | 0.666 | 0.171 | 0.665 | 0.866 |
| B25 | 0.081 | 0.402 | 0.831 | 0.099 | 0.403 | 0.833 | 0.559 | 0.099 | 0.533 |
| B26 | 0.523 | 0.846 | 0.499 | 0.484 | 0.822 | 0.500 | 0.864 | 0.376 | 0.700 |
| B27 | 0.152 | 0.659 | 0.866 | 0.173 | 0.671 | 0.866 | 0.326 | 0.302 | 0.886 |
| B28 | 0.596 | 0.103 | 0.533 | 0.560 | 0.092 | 0.532 | 0.714 | 0.737 | 0.553 |
| B29 | 0.875 | 0.383 | 0.700 | 0.866 | 0.382 | 0.699 | 0.020 | 0.013 | 0.719 |
| B30 | 0.305 | 0.305 | 0.886 | 0.324 | 0.311 | 0.886 | 0.482 | 0.961 | 0.968 |
| B31 | 0.750 | 0.750 | 0.553 | 0.711 | 0.731 | 0.553 | 0.868 | 0.381 | 0.635 |
| B32 | 0.029 | 0.029 | 0.719 | 0.018 | 0.021 | 0.719 | 0.176 | 0.670 | 0.802 |
| B33 | 0.436 | 0.948 | 0.967 | 0.482 | 0.967 | 0.968 | 0.014 | 0.016 | 0.612 |
| B34 | 0.882 | 0.393 | 0.634 | 0.869 | 0.387 | 0.635 | 0.321 | 0.306 | 0.779 |
| B35 | 0.158 | 0.670 | 0.800 | 0.176 | 0.677 | 0.801 | 0.627 | 0.596 | 0.946 |
| B36 | 0.402 | 0.081 | 0.831 | 0.015 | 0.021 | 0.612 | 0.127 | 0.478 | 0.332 |
| B37 | 0.846 | 0.523 | 0.499 | 0.322 | 0.310 | 0.779 | 0.433 | 0.767 | 0.166 |
| B38 | 0.125 | 0.805 | 0.665 | 0.629 | 0.600 | 0.946 | 0.223 | 0.238 | 0.279 |
| B39 | 0.142 | 0.463 | 0.331 | 0.128 | 0.471 | 0.332 | 0.530 | 0.528 | 0.112 |
| B40 | 0.419 | 0.739 | 0.165 | 0.435 | 0.760 | 0.166 | 0.917 | 0.948 | 0.446 |
| B41 | 0.662 | 0.151 | 0.134 | 0.224 | 0.232 | 0.279 | 0.676 | 0.163 | 0.135 |
| B42 | 0.108 | 0.596 | 0.467 | 0.531 | 0.521 | 0.112 | 0.062 | 0.583 | 0.468 |
| B43 | 0.386 | 0.874 | 0.300 | 0.918 | 0.942 | 0.446 | 0.368 | 0.874 | 0.302 |
| B44 | 0.794 | 0.794 | 0.053 | 0.675 | 0.157 | 0.135 | 0.830 | 0.807 | 0.053 |
| B45 | 0.239 | 0.239 | 0.386 | 0.062 | 0.577 | 0.468 | 0.218 | 0.242 | 0.386 |
| B46 | 0.515 | 0.515 | 0.219 | 0.369 | 0.867 | 0.302 | 0.524 | 0.531 | 0.219 |
| B47 | 0.948 | 0.441 | 0.033 | 0.831 | 0.815 | 0.053 | 0.985 | 0.445 | 0.033 |
| B48 | 0.392 | 0.885 | 0.366 | 0.219 | 0.235 | 0.386 | 0.373 | 0.879 | 0.366 |
| B49 | 0.669 | 0.161 | 0.200 | 0.525 | 0.525 | 0.219 | 0.680 | 0.168 | 0.200 |
| B50 | 0.463 | 0.142 | 0.331 | 0.988 | 0.453 | 0.033 | 0.448 | 0.144 | 0.333 |
| B51 | 0.739 | 0.419 | 0.165 | 0.373 | 0.873 | 0.366 | 0.755 | 0.433 | 0.166 |
| B52 | 0.053 | 0.053 | 0.083 | 0.681 | 0.162 | 0.200 | 0.078 | 0.062 | 0.084 |
| B53 | 0.502 | 0.502 | 0.415 | 0.449 | 0.138 | 0.333 | 0.463 | 0.480 | 0.417 |
| B54 | 0.777 | 0.777 | 0.249 | 0.756 | 0.427 | 0.166 | 0.769 | 0.769 | 0.250 |
| B55 | 0.803 | 0.127 | 0.335 | 0.075 | 0.053 | 0.084 | 0.792 | 0.120 | 0.334 |
| B56 | 0.079 | 0.403 | 0.168 | 0.464 | 0.473 | 0.417 | 0.099 | 0.410 | 0.167 |
| B57 | 0.361 | 0.684 | 0.000 | 0.770 | 0.763 | 0.250 | 0.403 | 0.691 | 0.000 |
| B58 | 0.151 | 0.662 | 0.134 | 0.793 | 0.114 | 0.334 | 0.172 | 0.679 | 0.134 |
| B59 | 0.596 | 0.108 | 0.467 | 0.099 | 0.403 | 0.167 | 0.559 | 0.099 | 0.468 |
| B60 | 0.874 | 0.386 | 0.300 | 0.407 | 0.695 | 0.000 | 0.865 | 0.389 | 0.301 |
| B61 | 0.306 | 0.306 | 0.114 | 0.173 | 0.671 | 0.134 | 0.327 | 0.316 | 0.114 |
| B62 | 0.753 | 0.753 | 0.446 | 0.560 | 0.092 | 0.468 | 0.711 | 0.738 | 0.447 |
| B63 | 0.030 | 0.030 | 0.281 | 0.866 | 0.382 | 0.301 | 0.017 | 0.027 | 0.281 |
| B64 | 0.441 | 0.948 | 0.033 | 0.324 | 0.311 | 0.114 | 0.482 | 0.961 | 0.032 |
| B65 | 0.885 | 0.392 | 0.366 | 0.711 | 0.731 | 0.447 | 0.869 | 0.394 | 0.365 |
| B66 | 0.161 | 0.669 | 0.200 | 0.018 | 0.021 | 0.281 | 0.175 | 0.683 | 0.198 |
| B67 | 0.034 | 0.034 | 0.391 | 0.482 | 0.967 | 0.032 | 0.015 | 0.028 | 0.388 |
| B68 | 0.310 | 0.310 | 0.224 | 0.869 | 0.387 | 0.365 | 0.322 | 0.316 | 0.221 |
| B69 | 0.589 | 0.589 | 0.056 | 0.176 | 0.677 | 0.199 | 0.627 | 0.594 | 0.054 |
| B70 | 0.403 | 0.079 | 0.168 | 0.015 | 0.021 | 0.388 | 0.417 | 0.066 | 0.832 |
| B71 | 0.684 | 0.361 | 0.000 | 0.322 | 0.310 | 0.221 | 0.111 | 0.777 | 0.666 |
| B72 | 0.127 | 0.803 | 0.335 | 0.629 | 0.600 | 0.054 | 0.723 | 0.359 | 0.000 |
| C1 | 0.040 | 0.040 | 0.613 | 0.419 | 0.095 | 0.833 | 0.739 | 0.024 | 0.000 |
| C2 | 0.316 | 0.316 | 0.780 | 0.804 | 0.514 | 0.500 | 0.125 | 0.443 | 0.668 |
| C3 | 0.593 | 0.593 | 0.948 | 0.112 | 0.806 | 0.666 | 0.432 | 0.732 | 0.834 |
| C4 | 0.228 | 0.228 | 0.280 | 0.419 | 0.095 | 0.168 | 0.805 | 0.520 | 0.500 |
| C5 | 0.504 | 0.504 | 0.113 | 0.727 | 0.387 | 0.000 | 0.419 | 0.101 | 0.168 |
| C6 | 0.951 | 0.951 | 0.448 | 0.112 | 0.806 | 0.334 | 0.112 | 0.812 | 0.334 |
| C7 | 0.888 | 0.888 | 0.896 | 0.913 | 0.909 | 0.895 | 0.923 | 0.912 | 0.897 |
| C8 | 0.338 | 0.338 | 0.564 | 0.301 | 0.330 | 0.562 | 0.300 | 0.338 | 0.563 |
| C9 | 0.612 | 0.612 | 0.731 | 0.606 | 0.620 | 0.729 | 0.616 | 0.624 | 0.730 |
| C10 | 0.196 | 0.196 | 0.935 | 0.234 | 0.204 | 0.937 | 0.244 | 0.208 | 0.938 |
| C11 | 0.644 | 0.644 | 0.602 | 0.622 | 0.625 | 0.604 | 0.632 | 0.627 | 0.604 |
| C12 | 0.921 | 0.921 | 0.768 | 0.929 | 0.914 | 0.770 | 0.939 | 0.918 | 0.771 |
| C13 | 0.900 | 0.900 | 0.102 | 0.913 | 0.909 | 0.105 | 0.912 | 0.917 | 0.104 |
| C14 | 0.348 | 0.348 | 0.435 | 0.301 | 0.330 | 0.438 | 0.300 | 0.336 | 0.438 |
| C15 | 0.623 | 0.623 | 0.268 | 0.606 | 0.620 | 0.271 | 0.605 | 0.626 | 0.271 |
| C16 | 0.206 | 0.206 | 0.064 | 0.234 | 0.204 | 0.064 | 0.244 | 0.206 | 0.063 |
| C17 | 0.656 | 0.656 | 0.396 | 0.622 | 0.625 | 0.397 | 0.621 | 0.632 | 0.397 |
| C18 | 0.932 | 0.932 | 0.231 | 0.929 | 0.914 | 0.230 | 0.928 | 0.920 | 0.230 |

Supplementary Table 4. The bond lengths (Å) in the icosahedral cages of the single crystal and 1-layer thick twinned B4C.

|  | Single crystal |  | Twin A1 |  | Twin S1 (layer A) |  | Twin S1 (layer B) |  | Twin R1 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Left side | Right side | Left side | Right side | Left side | Right side | Left side | Right side |  | Left side | Right side |
| 1 | 1.740 | 1.773 | 1.770 | 1.796 | 1.735 | 1.735 | 1.752 | 1.752 |  | 1.728 | 1.728 |
| 2 | 1.781 | 1.777 | 1.770 | 1.796 | 1.713 | 1.713 | 1.741 | 1.741 |  | 1.713 | 1.713 |
| 3 | 1.742 | 1.732 | 1.719 | 1.833 | 1.778 | 1.778 | 1.788 | 1.788 |  | 1.781 | 1.781 |
| 4 | 1.740 | 1.777 | 1.737 | 1.833 | 1.742 | 1.742 | 1.783 | 1.783 |  | 1.735 | 1.735 |
| 5 | 1.715 | 1.772 | 1.737 | 1.762 | 1.772 | 1.772 | 1.773 | 1.773 |  | 1.767 | 1.767 |
| 6 | 1.742 | 1.790 | 1.789 | 1.762 | 1.736 | 1.736 | 1.776 | 1.776 |  | 1.739 | 1.739 |
| 7 | 1.742 | 1.791 | 1.789 | 1.787 | 1.768 | 1.768 | 1.740 | 1.740 |  | 1.768 | 1.768 |
| 8 | 1.770 | 1.732 | 1.750 | 1.787 | 1.771 | 1.771 | 1.778 | 1.778 |  | 1.772 | 1.772 |
| 9 | 1.781 | 1.784 | 1.750 | 1.768 | 1.778 | 1.778 | 1.764 | 1.764 |  | 1.777 | 1.777 |
| 10 | 1.742 | 1.810 | 1.758 | 1.768 | 1.788 | 1.788 | 1.788 | 1.788 |  | 1.798 | 1.798 |
| 11 | 1.774 | 1.791 | 1.758 | 1.739 | 1.805 | 1.805 | 1.737 | 1.737 |  | 1.785 | 1.785 |
| 12 | 1.774 | 1.790 | 1.759 | 1.739 | 1.822 | 1.822 | 1.787 | 1.787 |  | 1.809 | 1.809 |
| 13 | 1.770 | 1.810 | 1.759 | 1.787 | 1.799 | 1.799 | 1.774 | 1.774 |  | 1.803 | 1.803 |
| mean | 1.755 | 1.779 | 1.757 | 1.781 | 1.770 | 1.770 | 1.768 | 1.768 |  | 1.767 | 1.767 |