Origins and Distribution of Hellenistic and Late Republican Transport Amphorae in the Dalmatian Region and its Implications for Adriatic Trade and Economy

Maja Miše 1

Patrick Sean Quinn 2

1 Institute of Archaeology, University College London, UK, mm2591@cam.ac.uk ORCID

2 Institute of Archaeology, University College London, UK

Supplement 2

The results of INAA geochemical compositions of all analysed samples of amphorae classifies according to type, archaeological context, and Fabric groups 1 – 7. All measurements are in ppm (particle per millimetre).

| Table 1A: Geochemical composition of analysed amphorae measured by INAA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample | Type | Site | Context | Fabric Group | As | La | Lu | Nd | Sm | U | Yb | Ce | Co | Cr | Cs | Eu | Fe | Hf | Ni |
| CG1 | Corinth B | Crveni Grm | Terre. | 2 | 10.76 | 36.95 | 0.44 | 33.25 | 6.56 | 2.56 | 3.23 | 77.89 | 27.38 | 302.82 | 7.20 | 1.32 | 49613.60 | 6.15 | 247.57 |
| CG2 | Corinth B | Crveni Grm | Terre. | 2 | 4.84 | 24.96 | 0.33 | 21.18 | 4.71 | 2.40 | 2.23 | 48.78 | 26.44 | 423.36 | 3.24 | 1.02 | 43196.80 | 3.22 | 253.8 |
| CG3 | Corinth B | Crveni Grm | Terre. | 3 | 10.96 | 34.74 | 0.40 | 30.92 | 6.14 | 1.86 | 2.62 | 75.76 | 29.03 | 318.77 | 6.58 | 1.27 | 52298.00 | 5.35 | 229.97 |
| CG4 | Corinth B | Crveni Grm | Terre. | 4 | 9.45 | 48.54 | 0.49 | 42.65 | 8.09 | 2.59 | 3.39 | 98.32 | 24.82 | 155.82 | 5.23 | 1.79 | 63736.50 | 3.81 | 71.01 |
| CG5 | Corinth B | Crveni Grm | Terre. | 3 | 11.39 | 35.33 | 0.40 | 28.36 | 6.29 | 2.41 | 2.78 | 75.51 | 27.77 | 315.91 | 7.11 | 1.28 | 52096.50 | 5.31 | 234.64 |
| CG6 | Corinth B | Crveni Grm | Terre. | Unass. | 0.01 | 28.04 | 0.33 | 24.40 | 5.33 | 2.17 | 2.78 | 54.32 | 29.02 | 498.28 | 5.11 | 1.11 | 48022.60 | 3.91 | 295.99 |
| GN1 | Corinth A' | Gnjilna | Marine | 5 | 104.40 | 29.26 | 0.41 | 27.69 | 5.79 | 8.33 | 2.17 | 57.08 | 48.31 | 260.99 | 3.86 | 1.07 | 43705.40 | 3.29 | 235.28 |
| GN2 | Corinth B | Gnjilna | Marine | 2 | 68.98 | 27.81 | 0.36 | 26.31 | 5.52 | 2.68 | 2.59 | 57.38 | 38.94 | 341.03 | 3.07 | 1.18 | 59050.00 | 3.75 | 235.35 |
| GN3 | Corinth B | Gnjilna | Marine | 2 | 44.04 | 24.79 | 0.31 | 22.93 | 4.72 | 2.40 | 2.46 | 53.82 | 38.31 | 323.41 | 6.13 | 1.16 | 58079.40 | 4.71 | 363.84 |
| GN4 | Corinth B | Gnjilna | Marine | 2 | 83.24 | 27.29 | 0.36 | 24.24 | 5.14 | 2.83 | 2.21 | 53.03 | 38.90 | 171.12 | 3.12 | 1.11 | 44995.70 | 2.92 | 180.74 |
| GN5 | Corinth B | Gnjilna | Marine | 2 | 148.84 | 29.29 | 0.44 | 26.21 | 5.60 | 3.22 | 2.36 | 56.32 | 62.62 | 185.94 | 1.82 | 1.19 | 50682.60 | 3.08 | 140.15 |
| GN6 | Corinth B | Gnjilna | Marine | 2 | 38.99 | 28.33 | 0.33 | 26.93 | 5.30 | 2.54 | 2.26 | 54.54 | 33.62 | 177.60 | 3.44 | 1.12 | 41978.30 | 2.99 | 157.34 |
| GN7 | Corinth B | Gnjilna | Marine | 2 | 27.77 | 19.67 | 0.28 | 18.93 | 3.95 | 1.91 | 1.88 | 41.05 | 28.06 | 420.20 | 2.10 | 0.85 | 36360.50 | 3.28 | 226.35 |
| GN8 | Corinth B | Gnjilna | Marine | Unass. | 59.29 | 19.78 | 0.27 | 16.43 | 3.99 | 2.14 | 2.08 | 40.63 | 33.79 | 338.52 | 1.12 | 0.88 | 38601.80 | 2.93 | 233.71 |
| GN9 | Corinth B | Gnjilna | Marine | 2 | 30.40 | 19.74 | 0.26 | 17.21 | 3.82 | 1.71 | 1.82 | 40.53 | 23.96 | 433.50 | 1.29 | 0.84 | 35614.10 | 3.05 | 214.38 |
| KOP1 | Corinth B | Kopila | Terre. | 4 | 12.99 | 49.67 | 0.56 | 43.71 | 8.32 | 3.01 | 4.04 | 96.14 | 24.77 | 158.76 | 2.58 | 1.89 | 66044.30 | 4.50 | 84.08 |
| KOP2 | Corinth B | Kopila | Terre. | 4 | 7.81 | 43.91 | 0.45 | 37.12 | 7.42 | 2.85 | 3.24 | 88.84 | 22.90 | 139.58 | 5.01 | 1.70 | 58588.90 | 3.85 | 48.03 |
| NAK1 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 6.89 | 31.64 | 0.30 | 23.03 | 5.49 | 2.77 | 2.23 | 64.15 | 14.20 | 117.52 | 6.70 | 1.17 | 38254.00 | 3.60 | 48.554 |
| NAK10 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 5.59 | 29.96 | 0.25 | 16.94 | 4.43 | 1.36 | 1.93 | 61.12 | 12.70 | 102.05 | 6.24 | 1.15 | 35134.80 | 4.15 | 37.2858 |
| NAK15 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 4.96 | 34.89 | 0.26 | 19.78 | 4.85 | 1.62 | 2.06 | 71.09 | 18.65 | 156.29 | 2.54 | 1.25 | 44299.50 | 4.18 | 46.6341 |
| NAK21 | Lamboglia 2 | Nak. Cave | Terre. | Unass. | 7.35 | 40.44 | 0.40 | 33.26 | 7.34 | 2.97 | 3.17 | 82.82 | 20.93 | 151.82 | 2.11 | 1.47 | 48867.10 | 5.08 | 62.3782 |
| NAK24 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 12.10 | 31.14 | 0.36 | 26.04 | 5.77 | 3.56 | 2.48 | 62.77 | 14.22 | 115.57 | 6.62 | 1.15 | 34349.60 | 4.37 | 35.8793 |
| NAK26 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 9.16 | 30.58 | 0.34 | 26.97 | 5.72 | 2.38 | 2.34 | 59.82 | 13.63 | 112.76 | 7.36 | 1.14 | 36945.00 | 3.59 | 41.7526 |
| NAK27 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 3.81 | 32.10 | 0.33 | 24.55 | 5.87 | 2.88 | 2.24 | 65.59 | 17.66 | 140.29 | 7.09 | 1.22 | 41713.70 | 4.07 | 63.388 |
| NAK29 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 7.47 | 32.29 | 0.36 | 27.51 | 6.10 | 2.56 | 2.16 | 65.29 | 14.78 | 143.23 | 6.31 | 1.17 | 40610.20 | 3.88 | 37.0213 |
| NAK3 | Lamboglia 2 | Nak. Cave | Terre. | Unass. | 2.29 | 22.84 | 0.26 | 18.84 | 4.09 | 1.44 | 2.23 | 47.90 | 25.73 | 453.98 | 6.05 | 0.98 | 44753.40 | 3.68 | 193.0334 |
| NAK30 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 8.00 | 35.33 | 0.40 | 28.48 | 6.78 | 2.77 | 2.58 | 70.46 | 14.26 | 129.96 | 7.83 | 1.28 | 40476.80 | 4.43 | 69.2422 |
| NAK31 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 7.22 | 37.31 | 0.41 | 33.12 | 6.97 | 2.97 | 2.70 | 75.79 | 17.95 | 131.96 | 5.76 | 1.31 | 42322.30 | 5.08 | 59.2832 |
| NAK33 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 7.75 | 31.82 | 0.38 | 25.41 | 6.10 | 2.36 | 2.45 | 63.13 | 11.56 | 93.40 | 4.98 | 1.21 | 35535.60 | 3.92 | 30.6616 |
| NAK34 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 9.63 | 36.36 | 0.42 | 29.91 | 7.03 | 2.92 | 3.13 | 75.13 | 16.69 | 107.16 | 6.58 | 1.29 | 37547.00 | 5.75 | 59.6965 |
| NAK4 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 3.50 | 31.86 | 0.34 | 24.95 | 5.69 | 3.32 | 1.98 | 65.16 | 14.17 | 144.26 | 7.34 | 1.12 | 40375.90 | 3.97 | 45.4954 |
| NAK5 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 4.87 | 30.34 | 0.37 | 27.99 | 5.60 | 3.32 | 2.13 | 61.41 | 14.99 | 142.59 | 6.86 | 1.11 | 37868.00 | 3.84 | 58.1378 |
| NAK6 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 9.59 | 34.99 | 0.41 | 30.37 | 6.43 | 3.23 | 2.76 | 70.50 | 15.64 | 146.18 | 7.01 | 1.26 | 41949.40 | 4.91 | 47.8624 |
| NAK7 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 11.49 | 29.09 | 0.34 | 26.11 | 5.55 | 2.12 | 2.35 | 57.09 | 12.13 | 104.85 | 3.88 | 1.11 | 32947.90 | 3.87 | 40.634 |
| NAK9 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 7.81 | 32.91 | 0.36 | 27.72 | 6.21 | 2.59 | 2.43 | 66.55 | 16.79 | 146.30 | 6.97 | 1.22 | 42184.30 | 4.25 | 24.3755 |
| POL1 | Lamboglia 2 | Polacisce | Marine | 1 | 39.53 | 30.13 | 0.40 | 26.61 | 5.45 | 2.86 | 2.37 | 63.33 | 14.26 | 118.31 | 6.48 | 1.10 | 38070.00 | 3.68 | 72.48 |
| POL10 | Lamboglia 2 | Polacisce | Marine | Unass. | 80.69 | 29.94 | 0.34 | 24.45 | 5.68 | 2.73 | 2.93 | 62.26 | 27.03 | 205.04 | 7.21 | 1.27 | 49611.90 | 4.30 | 111.51 |
| POL11 | Lamboglia 2 | Polacisce | Marine | 1 | 42.11 | 23.91 | 0.30 | 32.75 | 4.54 | 2.71 | 1.93 | 48.87 | 12.62 | 154.11 | 2.93 | 0.95 | 30713.20 | 3.38 | 55.69 |
| POL12 | Lamboglia 2 | Polacisce | Marine | Unass. | 45.25 | 36.16 | 0.45 | 32.13 | 6.71 | 5.44 | 2.53 | 78.92 | 22.37 | 173.10 | 2.32 | 1.27 | 47290.50 | 5.93 | 119.69 |
| POL13 | Lamboglia 2 | Polacisce | Marine | Unass. | 63.13 | 32.06 | 0.47 | 30.79 | 6.21 | 7.20 | 2.48 | 66.65 | 15.60 | 134.62 | 3.54 | 1.23 | 41460.70 | 3.70 | 73.38 |
| POL14 | Lamboglia 2 | Polacisce | Marine | 1 | 37.76 | 28.89 | 0.33 | 27.72 | 5.34 | 3.76 | 2.07 | 59.76 | 13.78 | 113.88 | 5.47 | 1.07 | 36564.50 | 3.66 | 61.78 |
| POL15 | Lamboglia 2 | Polacisce | Marine | Unass. | 65.77 | 31.26 | 0.54 | 30.62 | 6.28 | 10.97 | 2.45 | 66.37 | 13.61 | 112.78 | 4.82 | 1.13 | 36855.70 | 3.85 | 65.54 |
| POL16 | Lamboglia 2 | Polacisce | Marine | Unass. | 30.39 | 40.51 | 0.56 | 41.73 | 9.01 | 2.20 | 4.08 | 71.93 | 33.27 | 116.01 | 7.49 | 1.88 | 61224.90 | 4.37 | 146.43 |
| POL17 | Lamboglia 2 | Polacisce | Marine | 1 | 20.54 | 28.16 | 0.40 | 24.37 | 5.26 | 3.67 | 2.26 | 57.74 | 14.54 | 100.43 | 3.24 | 1.03 | 31006.90 | 4.27 | 104.6 |
| POL18 | Lamboglia 2 | Polacisce | Marine | 1 | 73.72 | 28.05 | 0.44 | 25.93 | 5.22 | 5.94 | 1.99 | 58.02 | 16.09 | 120.10 | 4.09 | 1.01 | 37680.80 | 3.15 | 77.46 |
| POL19 | Lamboglia 2 | Polacisce | Marine | Unass. | 39.76 | 21.65 | 0.38 | 19.68 | 4.40 | 4.98 | 2.13 | 46.26 | 24.53 | 470.67 | 4.87 | 0.91 | 47155.20 | 3.61 | 320.57 |
| POL19-1 | Lamboglia 2 | Polacisce | Marine | 1 | 28.88 | 27.77 | 0.36 | 28.32 | 4.98 | 4.20 | 1.88 | 56.75 | 17.20 | 134.67 | 6.41 | 0.99 | 37033.40 | 2.95 | 106.98 |
| POL19-2 | Lamboglia 2 | Polacisce | Marine | 1 | 24.38 | 25.54 | 0.32 | 20.25 | 4.61 | 4.48 | 1.88 | 53.72 | 15.21 | 123.23 | 5.89 | 0.95 | 34579.00 | 2.84 | 75.58 |
| POL2 | Lamboglia 2 | Polacisce | Marine | Unass. | 63.43 | 43.79 | 0.48 | 44.26 | 8.26 | 4.98 | 3.21 | 89.93 | 17.92 | 100.50 | 2.59 | 1.71 | 40321.10 | 6.68 | 75.76 |
| POL20 | Lamboglia 2 | Polacisce | Marine | Unass. | 10.71 | 37.83 | 0.34 | 30.89 | 6.51 | 2.94 | 2.52 | 80.89 | 14.94 | 93.97 | 4.49 | 1.39 | 41761.20 | 7.18 | 34.84 |
| POL21 | Lamboglia 2 | Polacisce | Marine | 1 | 19.12 | 27.49 | 0.29 | 22.99 | 4.77 | 2.32 | 2.02 | 56.61 | 16.46 | 136.03 | 5.29 | 1.00 | 37197.50 | 3.07 | 73 |
| POL22 | Lamboglia 2 | Polacisce | Marine | 1 | 15.81 | 28.93 | 0.35 | 25.01 | 5.30 | 2.52 | 2.43 | 59.94 | 14.70 | 99.12 | 2.81 | 1.09 | 31806.20 | 4.33 | 85.08 |
| POL3 | Lamboglia 2 | Polacisce | Marine | 1 | 36.00 | 26.81 | 0.46 | 25.56 | 5.33 | 4.74 | 2.21 | 56.50 | 19.01 | 145.30 | 3.01 | 1.13 | 44484.40 | 4.46 | 71.96 |
| POL4 | Lamboglia 2 | Polacisce | Marine | 1 | 21.78 | 29.38 | 0.31 | 26.85 | 5.31 | 3.15 | 2.10 | 59.53 | 15.87 | 121.02 | 5.19 | 1.06 | 36901.70 | 3.46 | 67.65 |
| POL5 | Lamboglia 2 | Polacisce | Marine | 1 | 24.29 | 28.03 | 0.31 | 21.69 | 4.98 | 2.58 | 1.97 | 59.20 | 15.94 | 120.18 | 4.47 | 1.02 | 38589.70 | 3.23 | 66.29 |
| POL6 | Lamboglia 2 | Polacisce | Marine | Unass. | 50.58 | 41.41 | 0.53 | 33.34 | 6.95 | 5.95 | 3.32 | 82.88 | 22.41 | 224.48 | 6.67 | 1.38 | 45758.40 | 5.46 | 123.02 |
| POL7 | Lamboglia 2 | Polacisce | Marine | 1 | 23.69 | 25.05 | 0.29 | 25.46 | 4.71 | 2.92 | 1.94 | 51.53 | 12.24 | 96.84 | 3.88 | 0.99 | 30047.00 | 3.61 | 51.36 |
| POL8 | Lamboglia 2 | Polacisce | Marine | 1 | 8.83 | 29.09 | 0.34 | 25.17 | 5.20 | 2.41 | 2.15 | 60.02 | 15.67 | 122.79 | 5.73 | 1.04 | 38099.20 | 3.39 | 52.89 |
| POL9 | Lamboglia 2 | Polacisce | Marine | 1 | 19.34 | 31.45 | 0.31 | 30.37 | 5.75 | 2.42 | 2.35 | 65.27 | 21.70 | 206.50 | 6.85 | 1.12 | 45745.00 | 3.41 | 136.56 |
| RAT1 | Corinth B | Rat | Terre. | 2 | 5.53 | 34.62 | 0.33 | 26.73 | 5.88 | 2.88 | 2.43 | 70.20 | 12.93 | 98.09 | 5.69 | 1.20 | 35801.00 | 4.41 | 75.32 |
| RAT2 | Corinth B | Rat | Terre. | 3 | 16.87 | 42.94 | 0.45 | 33.50 | 6.52 | 5.85 | 3.06 | 109.18 | 15.86 | 59.18 | 11.89 | 1.20 | 39174.60 | 8.32 | 12.3 |
| RAT3 | Corinth B | Rat | Terre. | 3 | 5.44 | 26.83 | 0.36 | 22.77 | 5.27 | 2.44 | 2.30 | 53.82 | 29.42 | 458.39 | 6.60 | 1.16 | 49013.50 | 3.82 | 248.48 |
| RAT4 | Corinth B | Rat | Terre. | 2 | 8.74 | 25.02 | 0.33 | 20.77 | 4.86 | 2.22 | 2.30 | 49.03 | 28.50 | 441.36 | 5.31 | 1.06 | 44206.90 | 3.42 | 265.36 |
| RAT5 | Corinth B | Rat | Terre. | 2 | 8.42 | 22.87 | 0.31 | 19.95 | 4.47 | 1.80 | 2.16 | 44.76 | 25.68 | 439.97 | 5.17 | 0.96 | 40294.70 | 3.05 | 203.2 |
| RAT6 | Corinth B | Rat | Terre. | 2 | 8.18 | 28.98 | 0.37 | 25.05 | 5.56 | 2.50 | 2.56 | 60.55 | 30.52 | 429.41 | 5.36 | 1.14 | 52149.10 | 4.08 | 287.48 |
| RAT7 | Corinth B | Rat | Terre. | 2 | 5.58 | 24.49 | 0.34 | 21.62 | 4.83 | 2.04 | 2.07 | 49.09 | 25.85 | 478.00 | 5.81 | 1.03 | 42760.50 | 3.75 | 230.65 |
| RAT8 | Corinth B | Rat | Terre. | 4 | 9.57 | 44.44 | 0.44 | 35.89 | 7.41 | 2.43 | 3.21 | 88.63 | 22.98 | 143.00 | 5.62 | 1.70 | 59230.50 | 3.83 | 44.06 |
| RES1 | Lamboglia 2 | Resnik | Terre. | 1 | 11.38 | 33.43 | 0.33 | 25.76 | 5.99 | 2.57 | 2.27 | 64.94 | 12.66 | 133.24 | 6.60 | 1.20 | 40112.20 | 4.02 | 26.7 |
| RES10 | Lamboglia 2 | Resnik | Terre. | 1 | 17.02 | 34.64 | 0.37 | 25.85 | 6.16 | 2.74 | 2.63 | 69.77 | 18.59 | 117.59 | 4.63 | 1.27 | 43272.00 | 4.24 | 56.55 |
| RES11 | Lamboglia 2 | Resnik | Terre. | Unass. | 13.19 | 35.26 | 0.40 | 29.71 | 6.42 | 2.67 | 3.01 | 70.84 | 17.00 | 152.93 | 4.68 | 1.29 | 38541.20 | 5.05 | 86.18 |
| RES12 | Lamboglia 2 | Resnik | Terre. | 1 | 13.24 | 32.72 | 0.33 | 27.91 | 5.79 | 2.40 | 2.42 | 66.76 | 17.83 | 140.57 | 6.02 | 1.16 | 42439.90 | 4.11 | 47.21 |
| RES13 | Lamboglia 2 | Resnik | Terre. | 1 | 12.72 | 34.58 | 0.43 | 26.60 | 6.26 | 3.08 | 2.83 | 71.16 | 16.94 | 156.64 | 6.98 | 1.22 | 37436.20 | 5.67 | 80.1 |
| RES14 | Lamboglia 2 | Resnik | Terre. | 1 | 6.74 | 32.45 | 0.37 | 24.79 | 5.88 | 2.83 | 2.44 | 65.98 | 17.51 | 172.33 | 6.20 | 1.21 | 41827.00 | 4.35 | 50.17 |
| RES15 | Lamboglia 2 | Resnik | Terre. | 1 | 10.92 | 33.34 | 0.38 | 26.63 | 6.03 | 1.86 | 2.59 | 69.61 | 17.78 | 89.56 | 3.98 | 1.24 | 39689.40 | 4.64 | 55.2 |
| RES16 | Lamboglia 2 | Resnik | Terre. | Unass. | 14.18 | 30.01 | 0.32 | 23.73 | 5.49 | 2.73 | 2.23 | 60.05 | 14.26 | 109.99 | 4.21 | 1.14 | 33978.20 | 3.70 | 41.44 |
| RES17 | Lamboglia 2 | Resnik | Terre. | 1 | 11.97 | 28.85 | 0.34 | 25.27 | 5.32 | 2.49 | 2.57 | 58.48 | 10.36 | 125.26 | 5.80 | 1.09 | 34311.50 | 3.82 | 29.51 |
| RES18 | Lamboglia 2 | Resnik | Terre. | Unass. | 11.15 | 28.40 | 0.34 | 25.45 | 5.44 | 1.79 | 2.54 | 56.69 | 20.85 | 196.94 | 3.24 | 1.20 | 44459.60 | 3.20 | 113.08 |
| RES19 | Lamboglia 2 | Resnik | Terre. | 1 | 11.14 | 31.34 | 0.36 | 28.05 | 5.63 | 2.38 | 2.59 | 61.12 | 14.89 | 118.07 | 2.15 | 1.17 | 36725.70 | 3.77 | 61.65 |
| RES2 | Lamboglia 2 | Resnik | Terre. | 1 | 9.92 | 33.34 | 0.36 | 28.39 | 6.08 | 2.32 | 2.51 | 66.74 | 16.51 | 132.92 | 4.89 | 1.21 | 41955.70 | 4.06 | 40.6 |
| RES20 | Lamboglia 2 | Resnik | Terre. | 1 | 6.35 | 34.90 | 0.40 | 29.53 | 6.30 | 3.03 | 2.69 | 70.52 | 18.43 | 160.37 | 3.96 | 1.29 | 46563.70 | 4.29 | 58.85 |
| RES21 | Lamboglia 2 | Resnik | Terre. | Unass. | 12.27 | 34.15 | 0.35 | 29.37 | 6.02 | 2.29 | 2.55 | 66.67 | 15.70 | 135.32 | 4.90 | 1.24 | 42227.30 | 3.75 | 47.87 |
| RES22 | Lamboglia 2 | Resnik | Terre. | 1 | 16.84 | 35.08 | 0.36 | 30.44 | 6.40 | 2.41 | 3.05 | 70.32 | 16.46 | 126.03 | 5.14 | 1.30 | 40856.60 | 4.77 | 48.73 |
| RES23 | Lamboglia 2 | Resnik | Terre. | 1 | 13.14 | 35.83 | 0.39 | 29.40 | 6.54 | 2.74 | 3.02 | 70.33 | 15.34 | 122.21 | 5.34 | 1.30 | 40353.50 | 4.98 | 55.79 |
| RES24 | Lamboglia 2 | Resnik | Terre. | 1 | 11.89 | 31.85 | 0.35 | 25.81 | 5.68 | 2.26 | 2.52 | 63.77 | 13.45 | 108.98 | 6.09 | 1.13 | 37081.70 | 4.46 | 32.76 |
| RES25 | Lamboglia 2 | Resnik | Terre. | 1 | 13.49 | 37.60 | 0.37 | 29.59 | 6.54 | 3.44 | 2.68 | 75.09 | 18.87 | 159.55 | 7.14 | 1.33 | 46700.40 | 4.21 | 53.62 |
| RES26 | Lamboglia 2 | Resnik | Terre. | Unass. | 13.02 | 28.81 | 0.31 | 24.68 | 5.25 | 2.24 | 2.12 | 56.23 | 15.09 | 97.82 | 3.40 | 1.06 | 32784.20 | 3.69 | 32.07 |
| RES27 | Lamboglia 2 | Resnik | Terre. | 1 | 10.90 | 34.00 | 0.37 | 29.21 | 6.14 | 2.77 | 2.75 | 70.72 | 16.83 | 164.32 | 3.71 | 1.19 | 45070.40 | 4.73 | 69.32 |
| RES28 | Lamboglia 2 | Resnik | Terre. | 1 | 11.25 | 29.89 | 0.33 | 25.13 | 5.35 | 2.75 | 2.37 | 57.11 | 13.27 | 125.77 | 3.80 | 1.10 | 38023.50 | 3.41 | 62.77 |
| RES29 | Lamboglia 2 | Resnik | Terre. | Unass. | 9.08 | 32.38 | 0.36 | 28.24 | 5.97 | 2.28 | 2.55 | 66.22 | 16.39 | 138.04 | 5.29 | 1.20 | 41621.40 | 4.06 | 54.11 |
| RES3 | Lamboglia 2 | Resnik | Terre. | 1 | 15.91 | 33.84 | 0.36 | 27.54 | 6.21 | 2.40 | 2.23 | 67.33 | 14.28 | 101.33 | 5.33 | 1.20 | 36157.40 | 4.58 | 46.02 |
| RES30 | Lamboglia 2 | Resnik | Terre. | 1 | 12.07 | 34.82 | 0.37 | 27.46 | 6.40 | 2.76 | 2.86 | 71.61 | 17.41 | 143.51 | 4.10 | 1.29 | 45039.90 | 4.46 | 44.77 |
| RES31 | Lamboglia 2 | Resnik | Terre. | Unass. | 10.33 | 34.55 | 0.39 | 30.01 | 6.31 | 2.99 | 2.81 | 70.97 | 17.42 | 139.99 | 4.17 | 1.28 | 45090.60 | 4.36 | 75.23 |
| RES32 | Lamboglia 2 | Resnik | Terre. | 1 | 6.32 | 34.94 | 0.36 | 29.90 | 6.11 | 2.57 | 2.60 | 69.67 | 17.95 | 149.32 | 5.00 | 1.27 | 45148.60 | 3.85 | 55.16 |
| RES33 | Lamboglia 2 | Resnik | Terre. | 1 | 10.42 | 30.01 | 0.32 | 26.65 | 5.35 | 2.78 | 2.42 | 59.73 | 14.48 | 93.82 | 4.24 | 1.12 | 36386.40 | 3.39 | 50.94 |
| RES34 | Lamboglia 2 | Resnik | Terre. | Unass. | 11.22 | 38.57 | 0.38 | 31.50 | 6.57 | 2.34 | 2.76 | 76.54 | 22.03 | 154.55 | 5.11 | 1.30 | 45545.10 | 4.56 | 96.06 |
| RES35 | Lamboglia 2 | Resnik | Terre. | 1 | 8.15 | 36.49 | 0.39 | 31.10 | 6.66 | 2.18 | 2.64 | 74.47 | 14.76 | 100.49 | 5.73 | 1.37 | 39294.10 | 4.53 | 63.69 |
| RES4 | Lamboglia 2 | Resnik | Terre. | 1 | 10.17 | 32.84 | 0.36 | 30.91 | 5.94 | 2.36 | 2.61 | 64.93 | 13.69 | 106.13 | 2.80 | 1.24 | 39886.10 | 3.85 | 55.81 |
| RES5 | Lamboglia 2 | Resnik | Terre. | Unass. | 15.88 | 35.60 | 0.37 | 30.15 | 6.47 | 3.02 | 2.96 | 70.76 | 14.12 | 120.45 | 6.27 | 1.26 | 39858.20 | 5.05 | 44.67 |
| RES6 | Lamboglia 2 | Resnik | Terre. | Unass. | 8.42 | 33.69 | 0.33 | 29.95 | 6.04 | 2.87 | 2.31 | 67.25 | 16.59 | 157.55 | 5.45 | 1.22 | 43406.70 | 4.06 | 53.12 |
| RES7 | Lamboglia 2 | Resnik | Terre. | Unass. | 7.55 | 26.81 | 0.36 | 21.82 | 4.99 | 3.33 | 2.43 | 56.39 | 31.84 | 414.73 | 7.25 | 1.14 | 52624.10 | 4.24 | 223.52 |
| RES8 | Lamboglia 2 | Resnik | Terre. | Unass. | 12.75 | 36.33 | 0.40 | 28.14 | 6.58 | 2.85 | 2.46 | 72.05 | 15.17 | 137.41 | 7.13 | 1.27 | 42478.80 | 4.29 | 57.7 |
| RES9 | Lamboglia 2 | Resnik | Terre. | Unass. | 10.82 | 34.89 | 0.41 | 27.62 | 6.21 | 3.17 | 2.30 | 68.66 | 16.22 | 145.43 | 5.52 | 1.23 | 36370.60 | 5.12 | 52.27 |
| SC1 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 27.82 | 26.25 | 0.44 | 21.28 | 5.07 | 6.34 | 2.20 | 53.60 | 12.65 | 86.89 | 3.08 | 0.97 | 31142.20 | 3.76 | 50.86 |
| SC10 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 26.67 | 28.32 | 0.32 | 25.14 | 5.16 | 3.10 | 2.23 | 58.97 | 14.33 | 67.32 | 2.00 | 1.03 | 32160.00 | 7.60 | 57.74 |
| SC11 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 12.42 | 35.52 | 0.34 | 30.10 | 6.04 | 2.17 | 2.24 | 75.37 | 13.78 | 94.38 | 5.19 | 1.31 | 37179.00 | 5.81 | 58.19 |
| SC12 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 65.60 | 32.76 | 0.49 | 30.84 | 6.30 | 5.19 | 2.74 | 64.98 | 28.47 | 248.67 | 4.90 | 1.31 | 49748.40 | 3.94 | 148.33 |
| SC13 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 16.71 | 35.37 | 0.36 | 31.82 | 6.24 | 3.09 | 2.69 | 76.26 | 13.51 | 89.32 | 4.36 | 1.36 | 37712.20 | 8.56 | 24.84 |
| SC2 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 36.15 | 26.84 | 0.46 | 29.82 | 5.35 | 8.18 | 2.10 | 56.29 | 13.09 | 105.55 | 3.61 | 0.97 | 32297.90 | 3.62 | 71.06 |
| SC3 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 40.48 | 28.40 | 0.44 | 26.42 | 5.49 | 6.03 | 2.34 | 60.48 | 15.41 | 106.88 | 4.06 | 1.06 | 35583.80 | 4.26 | 56.21 |
| SC4 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 47.65 | 28.01 | 0.31 | 25.35 | 5.25 | 2.05 | 2.21 | 58.05 | 24.05 | 107.36 | 5.36 | 1.08 | 46441.90 | 4.19 | 84.54 |
| SC5 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 40.71 | 26.76 | 0.29 | 23.95 | 5.01 | 3.10 | 2.04 | 55.39 | 16.81 | 98.28 | 4.53 | 1.01 | 37567.60 | 3.86 | 71.98 |
| SC6 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 14.09 | 40.89 | 0.43 | 34.93 | 6.96 | 2.84 | 2.76 | 84.84 | 14.77 | 107.30 | 5.77 | 1.51 | 46136.80 | 6.89 | 61.9 |
| SC7 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 13.23 | 27.22 | 0.32 | 26.94 | 4.89 | 2.64 | 1.98 | 56.97 | 11.82 | 69.03 | 2.16 | 1.07 | 30435.30 | 6.07 | 61.74 |
| SC8 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 34.67 | 39.69 | 0.49 | 32.63 | 7.01 | 4.85 | 2.63 | 85.03 | 15.09 | 108.66 | 5.29 | 1.49 | 42990.90 | 6.55 | 37.96 |
| SC9 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 27.24 | 39.17 | 0.38 | 32.92 | 6.92 | 2.98 | 2.77 | 81.68 | 15.75 | 97.44 | 4.99 | 1.44 | 45084.30 | 8.07 | 52.8 |
| SGP1 | Greco-Italic | Pharos | Terre. | 2 | 10.57 | 31.95 | 0.36 | 27.42 | 5.78 | 2.58 | 2.47 | 64.36 | 18.87 | 133.80 | 10.24 | 1.20 | 37686.90 | 4.21 | 99.35 |
| SGP10 | Corinth B | Pharos | Terre. | 2 | 13.00 | 24.34 | 0.30 | 25.48 | 4.75 | 2.15 | 2.21 | 48.41 | 24.26 | 383.98 | 4.83 | 1.03 | 44130.60 | 3.40 | 229.71 |
| SGP11 | Corinth B | Pharos | Terre. | 2 | 0.01 | 26.46 | 0.33 | 20.84 | 5.26 | 2.52 | 2.55 | 53.12 | 24.86 | 486.18 | 6.63 | 1.15 | 44474.10 | 3.86 | 227.98 |
| SGP12 | Hellenistic | Pharos | Terre. | 4 | 12.75 | 42.19 | 0.44 | 35.32 | 7.13 | 2.92 | 3.31 | 85.09 | 21.94 | 131.68 | 5.61 | 1.64 | 56648.20 | 3.81 | 74.55 |
| SGP13 | Hellenistic | Pharos | Terre. | 2 | 8.93 | 25.10 | 0.34 | 21.36 | 5.01 | 2.46 | 2.44 | 51.68 | 30.09 | 435.76 | 5.27 | 1.11 | 45932.80 | 3.67 | 230.6 |
| SGP14 | Hellenistic | Pharos | Terre. | 2 | 14.61 | 42.19 | 0.45 | 37.67 | 7.67 | 3.03 | 3.44 | 83.88 | 17.84 | 141.74 | 9.34 | 1.53 | 44946.20 | 6.13 | 78.38 |
| SGP15 | Hellenistic | Pharos | Terre. | 6 | 11.88 | 41.95 | 0.43 | 35.51 | 7.50 | 3.47 | 3.26 | 82.64 | 19.07 | 165.57 | 8.07 | 1.50 | 46040.60 | 5.47 | 82.7 |
| SGP16 | Hellenistic | Pharos | Terre. | 6 | 19.43 | 43.94 | 0.47 | 37.60 | 8.06 | 4.58 | 3.52 | 87.89 | 20.33 | 163.83 | 7.78 | 1.62 | 46783.20 | 6.20 | 97.07 |
| SGP17 | Corinth A' | Pharos | Terre. | 5 | 12.99 | 30.63 | 0.36 | 24.87 | 5.40 | 2.37 | 2.71 | 59.29 | 33.84 | 276.94 | 8.05 | 1.19 | 52977.60 | 3.08 | 225.44 |
| SGP18 | Greco-Italic | Pharos | Terre. | 2 | 40.54 | 34.24 | 0.35 | 28.55 | 6.04 | 4.28 | 2.75 | 68.51 | 19.00 | 164.15 | 8.18 | 1.26 | 48393.70 | 3.82 | 84.83 |
| SGP19 | Corinth B | Pharos | Terre. | 3 | 8.86 | 45.58 | 0.45 | 36.08 | 8.28 | 2.63 | 3.93 | 96.92 | 18.49 | 138.69 | 10.40 | 1.60 | 44357.00 | 7.27 | 76.03 |
| SGP2 | Corinth B | Pharos | Terre. | 2 | 10.09 | 25.03 | 0.32 | 20.19 | 4.96 | 2.28 | 2.41 | 50.82 | 29.93 | 409.70 | 5.42 | 1.09 | 44754.00 | 3.54 | 261.13 |
| SGP20 | Hellenistic | Pharos | Terre. | 7 | 6.17 | 45.61 | 0.46 | 39.07 | 8.22 | 3.05 | 3.73 | 95.73 | 32.80 | 316.04 | 10.62 | 1.74 | 56826.20 | 6.38 | 186.09 |
| SGP21 | Corinth B | Pharos | Terre. | 3 | 16.25 | 50.23 | 0.54 | 40.75 | 8.84 | 3.29 | 3.50 | 100.33 | 25.21 | 291.77 | 9.79 | 1.79 | 54229.70 | 7.16 | 143.92 |
| SGP22 | Hellenistic | Pharos | Terre. | 6 | 13.60 | 40.64 | 0.46 | 36.08 | 7.44 | 3.05 | 3.26 | 84.54 | 15.32 | 129.87 | 8.57 | 1.47 | 42849.60 | 6.40 | 38.76 |
| SGP23 | Greco-Italic | Pharos | Terre. | 2 | 12.29 | 27.05 | 0.30 | 22.03 | 4.98 | 2.96 | 2.04 | 52.50 | 12.12 | 89.73 | 3.91 | 0.98 | 30342.80 | 3.48 | 56.69 |
| SGP24 | Hellenistic | Pharos | Terre. | 2 | 8.16 | 35.38 | 0.35 | 29.87 | 6.14 | 3.03 | 2.21 | 70.39 | 13.58 | 86.08 | 5.28 | 1.20 | 35287.10 | 4.34 | 19.37 |
| SGP25 | Hellenistic | Pharos | Terre. | 4 | 10.40 | 47.55 | 0.44 | 39.56 | 7.94 | 2.86 | 3.11 | 96.49 | 23.88 | 149.21 | 6.83 | 1.72 | 61549.00 | 3.73 | 50.63 |
| SGP26 | Hellenistic | Pharos | Terre. | Unass. | 13.07 | 37.94 | 0.40 | 31.81 | 6.74 | 2.94 | 2.77 | 73.19 | 16.76 | 298.96 | 7.41 | 1.41 | 45530.40 | 5.81 | 103.62 |
| SGP27 | Lamboglia 2 | Pharos | Terre. | 1 | 13.42 | 31.24 | 0.36 | 26.50 | 5.79 | 2.68 | 2.29 | 63.59 | 13.20 | 95.25 | 5.15 | 1.11 | 35345.50 | 4.35 | 43.76 |
| SGP3 | Corinth B | Pharos | Terre. | 2 | 12.40 | 26.99 | 0.28 | 24.15 | 4.73 | 2.09 | 2.13 | 53.49 | 34.22 | 328.55 | 7.44 | 0.98 | 41767.20 | 3.68 | 377.9 |
| SGP4 | Corinth B | Pharos | Terre. | 2 | 10.48 | 22.67 | 0.31 | 19.76 | 4.64 | 1.61 | 2.45 | 49.51 | 30.24 | 347.93 | 14.06 | 1.10 | 51125.40 | 3.67 | 277.84 |
| SGP5 | Corinth B | Pharos | Terre. | 2 | 7.86 | 23.44 | 0.32 | 17.70 | 4.69 | 1.60 | 2.14 | 47.26 | 25.86 | 445.08 | 5.79 | 1.01 | 42805.10 | 3.37 | 233.6 |
| SGP6 | Corinth B | Pharos | Terre. | 3 | 17.52 | 47.59 | 0.50 | 38.99 | 8.43 | 3.65 | 3.43 | 99.03 | 26.22 | 310.22 | 9.60 | 1.75 | 52769.60 | 7.49 | 189.9 |
| SGP7 | Hellenistic | Pharos | Terre. | 7 | 31.22 | 68.92 | 0.59 | 53.42 | 11.01 | 4.27 | 4.27 | 138.30 | 22.93 | 246.11 | 15.68 | 2.24 | 61352.40 | 9.61 | 142.16 |
| SGP8 | Hellenistic | Pharos | Terre. | 4 | 9.98 | 45.68 | 0.46 | 36.67 | 7.74 | 3.14 | 3.54 | 92.28 | 23.69 | 142.55 | 6.91 | 1.67 | 59517.10 | 4.05 | 68 |
| SGP9 | Corinth B | Pharos | Terre. | 2 | 14.07 | 25.32 | 0.33 | 20.59 | 4.99 | 3.19 | 2.40 | 49.67 | 26.25 | 404.21 | 6.04 | 1.08 | 45374.80 | 3.42 | 228.95 |
| SOK1 | Corinth B | Sokol | Terre. | Unass. | 6.84 | 36.28 | 0.35 | 29.89 | 6.24 | 2.88 | 2.39 | 76.23 | 13.02 | 116.20 | 7.68 | 1.30 | 40495.90 | 4.77 | 45.02 |
| SOK10 | Corinth B | Sokol | Terre. | 2 | 6.63 | 31.07 | 0.42 | 28.20 | 6.08 | 2.48 | 2.62 | 66.27 | 33.16 | 474.99 | 3.81 | 1.25 | 54796.60 | 4.65 | 297.34 |
| SOK11 | Corinth B | Sokol | Terre. | 2 | 3.93 | 28.96 | 0.35 | 26.64 | 5.68 | 2.57 | 2.48 | 56.59 | 29.43 | 464.38 | 1.92 | 1.18 | 50896.20 | 3.77 | 254.7 |
| SOK12 | Hellenistic | Sokol | Terre. | 2 | 13.63 | 28.47 | 0.36 | 24.08 | 5.63 | 2.22 | 2.48 | 60.39 | 32.42 | 447.06 | 3.26 | 1.14 | 52092.60 | 4.16 | 306.48 |
| SOK13 | Corinth B | Sokol | Terre. | 2 | 11.07 | 28.69 | 0.37 | 27.21 | 5.62 | 2.62 | 2.38 | 60.55 | 30.02 | 419.25 | 3.74 | 1.15 | 51281.60 | 4.40 | 306.68 |
| SOK14 | Hellenistic | Sokol | Terre. | 2 | 4.73 | 27.41 | 0.35 | 26.32 | 5.37 | 2.04 | 2.40 | 55.62 | 27.55 | 529.87 | 2.28 | 1.12 | 47385.80 | 4.40 | 178.64 |
| SOK15 | Hellenistic | Sokol | Terre. | 2 | 9.56 | 41.28 | 0.41 | 35.80 | 7.51 | 3.11 | 3.01 | 84.13 | 16.80 | 148.49 | 3.47 | 1.45 | 46437.30 | 5.60 | 103.23 |
| SOK2 | Corinth B | Sokol | Terre. | 6 | 12.40 | 38.52 | 0.40 | 33.36 | 6.85 | 2.58 | 3.05 | 77.88 | 18.21 | 170.82 | 3.99 | 1.40 | 48454.90 | 4.47 | 67.72 |
| SOK3 | Corinth B | Sokol | Terre. | 2 | 3.90 | 28.65 | 0.38 | 24.71 | 5.61 | 2.31 | 2.42 | 56.41 | 30.07 | 471.03 | 2.32 | 1.20 | 51230.10 | 3.82 | 228.42 |
| SOK4 | Corinth B | Sokol | Terre. | Unass. | 4.50 | 27.90 | 0.37 | 24.37 | 5.38 | 2.18 | 2.46 | 56.48 | 25.91 | 504.44 | 2.13 | 1.16 | 47641.10 | 4.47 | 242.2 |
| SOK5 | Corinth B | Sokol | Terre. | 2 | 4.59 | 29.12 | 0.36 | 25.20 | 5.65 | 2.00 | 2.23 | 58.21 | 32.80 | 495.39 | 1.64 | 1.22 | 52495.30 | 3.96 | 266.37 |
| SOK6 | Greco-Italic | Sokol | Terre. | 2 | 8.39 | 29.59 | 0.34 | 24.92 | 5.39 | 2.11 | 2.33 | 57.32 | 12.84 | 113.85 | 4.26 | 1.10 | 34568.20 | 3.51 | 48.88 |
| SOK7 | Corinth B | Sokol | Terre. | 2 | 4.64 | 26.78 | 0.39 | 23.85 | 5.18 | 1.82 | 2.31 | 53.80 | 28.65 | 448.88 | 5.53 | 1.12 | 47158.20 | 3.75 | 248.82 |
| SOK8 | Hellenistic | Sokol | Terre. | 6 | 7.66 | 45.24 | 0.50 | 39.24 | 8.11 | 3.37 | 3.61 | 92.35 | 22.15 | 178.74 | 2.98 | 1.60 | 49952.30 | 6.11 | 121.63 |
| SOK9 | Corinth B | Sokol | Terre. | 2 | 5.14 | 27.22 | 0.35 | 24.91 | 5.35 | 1.64 | 2.33 | 54.45 | 29.07 | 494.05 | 2.39 | 1.18 | 47114.60 | 4.04 | 252.94 |
| STI1 | Corinth B | Stine | Terre. | 3 | 14.44 | 61.85 | 0.58 | 55.82 | 10.59 | 2.79 | 4.46 | 119.89 | 26.97 | 328.58 | 8.09 | 2.19 | 55575.50 | 9.30 | 202.27 |
| STI2 | Corinth B | Stine | Terre. | 3 | 8.34 | 52.27 | 0.55 | 44.32 | 8.68 | 3.06 | 4.00 | 103.82 | 23.45 | 337.37 | 8.30 | 1.72 | 50347.50 | 10.21 | 164.39 |
| VIC1 | Corinth B | Vilina Cave | Terre. | 4 | 5.71 | 44.05 | 0.44 | 37.26 | 7.47 | 3.44 | 3.21 | 87.65 | 21.14 | 138.25 | 6.49 | 1.66 | 58011.10 | 3.77 | 81.94 |
| VIC10 | Corinth B | Vilina Cave | Terre. | 2 | 3.87 | 26.28 | 0.34 | 22.73 | 5.11 | 2.64 | 2.62 | 51.28 | 28.00 | 430.52 | 6.01 | 1.02 | 45777.40 | 3.64 | 205.54 |
| VIC11 | Corinth B | Vilina Cave | Terre. | 2 | 4.90 | 21.78 | 0.31 | 21.18 | 4.37 | 2.95 | 2.00 | 45.23 | 23.92 | 442.96 | 5.56 | 0.89 | 46086.70 | 3.68 | 217.76 |
| VIC12 | Corinth B | Vilina Cave | Terre. | 2 | 3.54 | 26.67 | 0.34 | 22.73 | 5.20 | 2.52 | 2.19 | 52.98 | 27.16 | 470.04 | 6.03 | 1.08 | 47022.40 | 3.78 | 244.34 |
| VIC13 | Corinth B | Vilina Cave | Terre. | 2 | 4.78 | 25.01 | 0.34 | 22.19 | 4.96 | 2.25 | 2.26 | 50.19 | 25.48 | 436.49 | 5.69 | 1.02 | 43824.20 | 3.59 | 235.02 |
| VIC14 | Corinth B | Vilina Cave | Terre. | 2 | 3.35 | 26.33 | 0.34 | 22.58 | 5.12 | 2.39 | 2.43 | 51.80 | 27.19 | 414.16 | 6.08 | 1.08 | 46947.50 | 3.59 | 229.03 |
| VIC15 | Corinth B | Vilina Cave | Terre. | 2 | 6.11 | 28.59 | 0.38 | 23.99 | 5.72 | 2.66 | 2.52 | 57.41 | 29.84 | 533.72 | 3.91 | 1.19 | 50321.80 | 4.18 | 258.37 |
| VIC16 | Corinth B | Vilina Cave | Terre. | 2 | 4.43 | 23.75 | 0.33 | 21.54 | 4.62 | 2.05 | 2.18 | 47.59 | 24.40 | 437.80 | 5.33 | 0.97 | 41482.90 | 3.42 | 212.45 |
| VIC17 | Corinth B | Vilina Cave | Terre. | Unass. | 2.36 | 24.87 | 0.35 | 22.97 | 4.98 | 2.62 | 2.15 | 50.54 | 28.03 | 420.81 | 5.58 | 1.06 | 46810.80 | 3.80 | 247.07 |
| VIC18 | Corinth B | Vilina Cave | Terre. | 2 | 3.95 | 23.24 | 0.30 | 21.76 | 4.41 | 2.34 | 1.90 | 45.50 | 24.72 | 400.30 | 5.00 | 0.94 | 39046.70 | 3.12 | 209 |
| VIC19 | Corinth B | Vilina Cave | Terre. | 2 | 3.25 | 25.56 | 0.34 | 25.56 | 5.16 | 2.28 | 2.43 | 51.57 | 28.11 | 458.22 | 5.54 | 1.09 | 48011.90 | 3.80 | 230.09 |
| VIC2 | Corinth B | Vilina Cave | Terre. | 2 | 6.84 | 24.78 | 0.32 | 24.98 | 4.94 | 2.16 | 2.26 | 50.73 | 25.45 | 438.50 | 5.00 | 1.03 | 45387.20 | 3.54 | 235.73 |
| VIC20 | Corinth B | Vilina Cave | Terre. | 2 | 3.41 | 26.67 | 0.36 | 23.31 | 5.31 | 2.64 | 2.69 | 54.55 | 29.35 | 496.51 | 5.53 | 1.11 | 49976.90 | 3.84 | 253.56 |
| VIC21 | Corinth B | Vilina Cave | Terre. | Unass. | 3.38 | 24.72 | 0.35 | 21.74 | 4.86 | 2.75 | 2.07 | 48.57 | 26.32 | 418.55 | 5.57 | 1.01 | 42639.00 | 3.28 | 220.56 |
| VIC22 | Corinth B | Vilina Cave | Terre. | 2 | 3.19 | 25.06 | 0.32 | 24.88 | 4.93 | 2.25 | 2.38 | 49.35 | 27.77 | 441.46 | 5.76 | 1.03 | 43206.50 | 3.60 | 257.97 |
| VIC23 | Corinth B | Vilina Cave | Terre. | 2 | 3.58 | 21.32 | 0.35 | 19.32 | 4.29 | 2.76 | 2.22 | 42.55 | 20.40 | 433.12 | 5.58 | 0.87 | 39432.00 | 3.71 | 186.39 |
| VIC24 | Corinth B | Vilina Cave | Terre. | 2 | 6.85 | 26.36 | 0.34 | 24.30 | 5.06 | 2.60 | 2.33 | 50.27 | 16.11 | 428.70 | 2.55 | 1.03 | 42542.60 | 3.42 | 113.2 |
| VIC25 | Corinth B | Vilina Cave | Terre. | 2 | 4.59 | 24.92 | 0.34 | 20.70 | 4.91 | 1.81 | 2.59 | 49.90 | 26.42 | 451.27 | 5.76 | 1.01 | 43347.40 | 3.67 | 231.8 |
| VIC26 | Corinth B | Vilina Cave | Terre. | 2 | 7.81 | 25.96 | 0.35 | 24.18 | 5.11 | 2.38 | 2.31 | 51.67 | 27.96 | 453.73 | 5.49 | 1.08 | 45519.20 | 3.73 | 240.29 |
| VIC27 | Corinth B | Vilina Cave | Terre. | 2 | 5.82 | 26.33 | 0.34 | 24.07 | 5.36 | 1.91 | 2.21 | 53.90 | 26.33 | 459.40 | 3.71 | 1.13 | 48190.30 | 3.74 | 178.6461 |
| VIC28 | Corinth B | Vilina Cave | Terre. | 2 | 4.95 | 23.77 | 0.34 | 20.98 | 5.03 | 2.27 | 2.15 | 50.39 | 28.64 | 407.13 | 4.58 | 1.06 | 45064.00 | 3.34 | 162.5899 |
| VIC29 | Corinth B | Vilina Cave | Terre. | 2 | 3.09 | 22.69 | 0.31 | 16.95 | 4.54 | 2.41 | 1.88 | 47.23 | 24.89 | 437.27 | 5.50 | 0.98 | 42124.00 | 3.59 | 151.7398 |
| VIC3 | Corinth B | Vilina Cave | Terre. | 2 | 3.45 | 24.95 | 0.34 | 21.83 | 5.00 | 2.54 | 2.59 | 50.19 | 22.60 | 463.77 | 5.22 | 1.04 | 44474.80 | 3.82 | 203.48 |
| VIC30 | Corinth B | Vilina Cave | Terre. | 6 | 3.86 | 26.45 | 0.33 | 24.05 | 5.17 | 2.45 | 2.28 | 53.43 | 22.55 | 479.25 | 4.83 | 1.07 | 45053.60 | 3.74 | 132.4713 |
| VIC31 | Corinth B | Vilina Cave | Terre. | 6 | 9.24 | 32.47 | 0.33 | 26.08 | 6.03 | 2.45 | 2.34 | 64.03 | 14.36 | 121.33 | 6.78 | 1.18 | 36747.90 | 4.00 | 49.8992 |
| VIC32 | Corinth B | Vilina Cave | Terre. | 2 | 7.54 | 26.22 | 0.35 | 23.26 | 5.35 | 2.58 | 2.31 | 55.80 | 28.55 | 409.63 | 5.82 | 1.05 | 47011.80 | 3.78 | 171.8641 |
| VIC4 | Corinth B | Vilina Cave | Terre. | 2 | 4.53 | 24.75 | 0.33 | 22.55 | 4.81 | 2.09 | 2.14 | 49.72 | 22.23 | 494.58 | 4.50 | 1.03 | 47258.80 | 3.90 | 217.24 |
| VIC5 | Corinth B | Vilina Cave | Terre. | 2 | 4.19 | 25.98 | 0.34 | 22.94 | 5.05 | 2.53 | 2.26 | 51.81 | 24.12 | 450.10 | 6.66 | 1.06 | 47342.50 | 3.66 | 236.49 |
| VIC6 | Corinth B | Vilina Cave | Terre. | 2 | 4.36 | 23.29 | 0.34 | 19.91 | 4.62 | 2.33 | 2.09 | 48.04 | 25.72 | 469.21 | 5.81 | 0.96 | 45988.10 | 3.60 | 182.29 |
| VIC7 | Corinth B | Vilina Cave | Terre. | 2 | 8.30 | 24.09 | 0.35 | 19.08 | 4.79 | 2.37 | 2.25 | 47.79 | 22.08 | 479.85 | 5.99 | 0.98 | 44779.20 | 3.72 | 226.99 |
| VIC8 | Corinth B | Vilina Cave | Terre. | 2 | 1.96 | 25.09 | 0.32 | 21.75 | 4.80 | 2.27 | 2.08 | 50.38 | 22.37 | 455.61 | 6.35 | 1.01 | 45717.80 | 3.52 | 210.43 |
| VIC9 | Corinth B | Vilina Cave | Terre. | 2 | 3.41 | 25.41 | 0.34 | 21.65 | 4.90 | 2.80 | 2.20 | 49.45 | 23.28 | 417.38 | 6.08 | 1.06 | 44658.80 | 3.41 | 215.67 |
| VS1 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 12.74 | 26.02 | 0.30 | 23.68 | 4.90 | 2.34 | 2.05 | 51.79 | 11.89 | 104.29 | 5.04 | 1.00 | 30276.40 | 3.34 | 32.67 |
| VS10 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 34.00 | 28.98 | 0.33 | 24.45 | 5.39 | 3.27 | 1.91 | 58.54 | 14.09 | 104.17 | 4.36 | 1.04 | 31927.40 | 4.28 | 44.67 |
| VS11 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 15.97 | 26.81 | 0.31 | 24.40 | 5.13 | 2.68 | 2.11 | 52.04 | 14.62 | 106.85 | 5.07 | 1.01 | 32003.60 | 3.54 | 45.13 |
| VS12 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 20.13 | 33.22 | 0.36 | 28.58 | 6.10 | 2.89 | 2.48 | 66.71 | 14.54 | 122.80 | 7.97 | 1.19 | 39295.10 | 4.71 | 42.17 |
| VS13 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 14.99 | 29.60 | 0.34 | 24.45 | 5.45 | 2.48 | 2.08 | 57.11 | 14.03 | 97.92 | 2.38 | 1.09 | 33980.10 | 3.94 | 49.58 |
| VS14 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 28.46 | 28.21 | 0.34 | 24.69 | 5.38 | 4.15 | 2.13 | 56.60 | 14.28 | 102.41 | 3.41 | 1.04 | 33543.80 | 3.58 | 43.45 |
| VS15 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 14.50 | 27.36 | 0.35 | 24.64 | 5.24 | 4.18 | 2.27 | 54.68 | 12.40 | 115.36 | 2.39 | 1.04 | 30780.00 | 3.57 | 26.38 |
| VS16 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 46.39 | 25.56 | 0.38 | 23.30 | 5.19 | 8.70 | 1.77 | 51.28 | 13.96 | 97.99 | 4.27 | 0.95 | 28474.80 | 3.15 | 57.68 |
| VS17 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 18.23 | 28.08 | 0.31 | 27.00 | 5.19 | 2.36 | 2.05 | 53.87 | 12.95 | 108.77 | 4.46 | 1.03 | 32616.30 | 3.44 | 64.61 |
| VS18 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 17.87 | 27.31 | 0.28 | 24.18 | 5.05 | 2.36 | 2.10 | 53.45 | 11.74 | 102.52 | 3.67 | 0.99 | 31599.90 | 3.69 | 32.86 |
| VS19 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 28.43 | 28.33 | 0.29 | 25.37 | 5.31 | 2.98 | 1.98 | 56.49 | 13.00 | 105.12 | 4.66 | 1.02 | 30759.60 | 4.08 | 35.2 |
| VS2 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 15.74 | 27.00 | 0.30 | 23.13 | 4.96 | 2.47 | 2.05 | 52.69 | 12.18 | 95.43 | 2.88 | 1.00 | 31849.80 | 3.52 | 45.49 |
| VS20 | Lamboglia | Vela Svitnja | Marine | 1 | 14.54 | 24.44 | 0.29 | 20.72 | 4.49 | 2.34 | 1.86 | 47.43 | 12.65 | 95.80 | 4.52 | 0.88 | 30060.08 | 2.57 | 0.00 |
| VS21 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 44.47 | 28.46 | 0.35 | 24.96 | 5.39 | 3.10 | 2.12 | 55.70 | 18.26 | 118.79 | 5.31 | 1.05 | 37045.90 | 3.59 | 75.51 |
| VS22 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 32.87 | 31.18 | 0.34 | 28.67 | 5.77 | 2.68 | 2.15 | 61.63 | 21.30 | 126.82 | 5.27 | 1.15 | 43126.70 | 3.99 | 76.29 |
| VS23 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 58.99 | 34.42 | 0.41 | 31.63 | 6.43 | 4.40 | 2.58 | 69.32 | 27.55 | 132.41 | 5.30 | 1.21 | 42065.20 | 4.56 | 76.83 |
| VS24 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 12.17 | 30.15 | 0.33 | 24.80 | 5.49 | 2.00 | 2.32 | 59.56 | 14.23 | 93.32 | 5.32 | 1.08 | 28525.60 | 4.27 | 47.87 |
| VS25 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 14.27 | 26.24 | 0.32 | 23.33 | 5.10 | 3.32 | 2.00 | 52.10 | 12.93 | 113.62 | 5.48 | 0.98 | 30120.00 | 3.40 | 49.11 |
| VS26 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 22.01 | 26.78 | 0.30 | 23.88 | 4.94 | 2.40 | 2.15 | 52.93 | 12.21 | 87.79 | 4.14 | 1.00 | 31476.20 | 3.29 | 51.25 |
| VS27 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 31.68 | 25.17 | 0.32 | 24.08 | 4.80 | 2.35 | 1.98 | 49.15 | 16.96 | 99.85 | 2.61 | 0.91 | 31289.10 | 3.38 | 60.64 |
| VS28 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 16.26 | 25.94 | 0.27 | 22.98 | 4.76 | 2.31 | 2.05 | 51.12 | 12.03 | 69.02 | 2.28 | 0.93 | 27674.20 | 3.24 | 34.29 |
| VS29 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 28.41 | 28.43 | 0.37 | 25.16 | 5.56 | 9.12 | 2.18 | 57.74 | 14.09 | 112.47 | 3.39 | 1.04 | 35033.60 | 3.23 | 46.11 |
| VS3 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 16.16 | 26.77 | 0.33 | 23.74 | 5.10 | 4.74 | 1.80 | 54.52 | 12.48 | 97.10 | 4.37 | 0.95 | 30259.60 | 3.74 | 30.35 |
| VS30 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 22.05 | 29.31 | 0.33 | 26.94 | 5.45 | 3.24 | 2.35 | 57.77 | 12.92 | 94.46 | 5.63 | 1.08 | 35798.80 | 3.78 | 65.56 |
| VS31 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 12.38 | 23.66 | 0.28 | 23.42 | 4.54 | 2.46 | 1.96 | 45.62 | 10.40 | 99.78 | 4.91 | 0.89 | 27326.10 | 2.99 | 34.68 |
| VS32 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 23.16 | 23.94 | 0.29 | 23.63 | 4.49 | 2.06 | 1.70 | 47.27 | 13.33 | 80.33 | 1.84 | 0.88 | 29445.20 | 3.18 | 57.65 |
| VS4 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 33.60 | 26.03 | 0.32 | 21.58 | 4.90 | 2.27 | 2.27 | 50.99 | 13.26 | 99.45 | 2.42 | 1.00 | 32518.60 | 3.62 | 55.42 |
| VS5 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 13.16 | 26.33 | 0.32 | 24.37 | 4.96 | 2.80 | 1.91 | 51.79 | 13.45 | 102.69 | 1.15 | 1.00 | 29642.80 | 3.45 | 57.76 |
| VS6 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 26.78 | 24.68 | 0.32 | 22.14 | 4.77 | 4.03 | 1.77 | 48.53 | 11.40 | 104.96 | 3.74 | 0.91 | 28982.80 | 3.11 | 60.81 |
| VS7 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 17.61 | 26.63 | 0.32 | 23.99 | 5.07 | 2.74 | 2.22 | 52.86 | 13.73 | 107.62 | 4.80 | 1.00 | 32242.70 | 3.44 | 26.83 |
| VS8 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 22.01 | 32.65 | 0.36 | 30.23 | 6.05 | 3.46 | 2.07 | 65.05 | 15.45 | 129.52 | 6.91 | 1.18 | 39999.80 | 3.86 | 99.5 |
| VS9 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 11.05 | 24.88 | 0.30 | 22.21 | 4.79 | 2.27 | 1.86 | 50.97 | 14.50 | 96.14 | 3.40 | 0.97 | 29479.50 | 3.55 | 37.21 |
| ZEM1 | Corinth B | Zemunik | Terre. | 4 | 4.43 | 41.62 | 0.48 | 35.09 | 7.08 | 2.89 | 3.27 | 83.61 | 21.81 | 132.99 | 6.16 | 1.62 | 55797.30 | 4.00 | 73.96 |
| ZEM2 | Corinth B | Zemunik | Terre. | 2 | 1.80 | 24.72 | 0.33 | 20.80 | 4.80 | 2.15 | 2.22 | 49.44 | 25.09 | 487.24 | 6.13 | 1.03 | 43738.20 | 3.49 | 245.84 |
| ZEM3 | Corinth B | Zemunik | Terre. | 4 | 9.82 | 44.55 | 0.44 | 39.33 | 7.44 | 3.19 | 2.90 | 90.86 | 22.77 | 137.60 | 6.54 | 1.66 | 57785.20 | 3.99 | 59.88 |
| ZIR1 | Corinth B | Zirje | Marine | 2 | 27.25 | 19.94 | 0.27 | 18.17 | 4.01 | 1.68 | 1.97 | 41.10 | 23.38 | 378.35 | 1.95 | 0.87 | 36254.60 | 2.84 | 204.5 |
| ZIR10 | Corinth B | Zirje | Marine | Unass. | 98.25 | 36.19 | 0.42 | 35.05 | 7.12 | 3.23 | 2.90 | 61.59 | 29.37 | 292.49 | 6.84 | 1.52 | 46059.40 | 3.50 | 241.68 |
| ZIR11 | Corinth B | Zirje | Marine | 3 | 15.40 | 43.27 | 0.42 | 38.23 | 7.41 | 2.84 | 3.13 | 86.39 | 24.65 | 318.73 | 3.29 | 1.47 | 45911.40 | 9.10 | 171.3 |
| ZIR12 | Corinth B | Zirje | Marine | 3 | 95.04 | 39.14 | 0.62 | 36.57 | 7.94 | 18.78 | 3.24 | 81.35 | 27.33 | 302.49 | 5.78 | 1.36 | 45067.60 | 6.82 | 210.74 |
| ZIR13 | Corinth B | Zirje | Marine | 3 | 86.97 | 47.66 | 0.61 | 41.32 | 9.27 | 17.11 | 3.47 | 97.29 | 27.29 | 284.92 | 5.98 | 1.71 | 48714.50 | 6.80 | 202.03 |
| ZIR14 | Corinth B | Zirje | Marine | Unass. | 40.88 | 37.00 | 0.42 | 31.75 | 6.60 | 2.43 | 3.16 | 76.13 | 25.73 | 302.96 | 3.42 | 1.33 | 45278.70 | 6.92 | 160.06 |
| ZIR15 | Corinth B | Zirje | Marine | 3 | 69.86 | 35.20 | 0.44 | 32.99 | 6.61 | 6.79 | 2.72 | 72.41 | 24.33 | 283.40 | 3.22 | 1.25 | 42879.10 | 6.34 | 215.59 |
| ZIR16 | Corinth B | Zirje | Marine | 2 | 97.55 | 23.37 | 0.32 | 19.65 | 4.53 | 2.56 | 2.14 | 48.81 | 27.67 | 276.10 | 1.12 | 0.94 | 54066.10 | 2.92 | 248.22 |
| ZIR17 | Corinth B | Zirje | Marine | 3 | 49.36 | 42.68 | 0.58 | 38.96 | 8.24 | 13.77 | 3.43 | 87.84 | 23.41 | 298.55 | 4.65 | 1.50 | 45235.20 | 9.38 | 132.72 |
| ZIR18 | Corinth B | Zirje | Marine | 3 | 60.00 | 39.65 | 0.48 | 37.24 | 7.16 | 3.85 | 3.24 | 80.55 | 28.32 | 319.75 | 3.19 | 1.42 | 48279.30 | 7.07 | 199.62 |
| ZIR19 | Corinth B | Zirje | Marine | Unass. | 28.12 | 18.88 | 0.27 | 16.34 | 3.73 | 2.52 | 1.77 | 37.86 | 20.60 | 380.60 | 2.20 | 0.81 | 34508.40 | 2.95 | 202.69 |
| ZIR2 | Corinth B | Zirje | Marine | 3 | 23.64 | 44.35 | 0.46 | 35.31 | 7.71 | 2.22 | 3.48 | 87.44 | 23.10 | 278.47 | 6.27 | 1.50 | 45896.80 | 8.21 | 127.55 |
| ZIR20 | Corinth B | Zirje | Marine | Unass. | 32.78 | 17.93 | 0.23 | 19.23 | 3.65 | 3.05 | 1.74 | 35.86 | 17.44 | 389.79 | 0.65 | 0.73 | 28881.60 | 2.77 | 179.46 |
| ZIR21 | Corinth B | Zirje | Marine | Unass. | 30.89 | 37.98 | 0.42 | 34.87 | 6.76 | 2.83 | 3.18 | 78.24 | 22.69 | 353.52 | 1.47 | 1.34 | 42490.10 | 10.24 | 164.16 |
| ZIR22 | Corinth B | Zirje | Marine | 3 | 31.10 | 50.74 | 0.54 | 40.14 | 9.08 | 7.17 | 3.31 | 96.98 | 24.90 | 258.24 | 6.96 | 1.78 | 50655.70 | 6.39 | 161.31 |
| ZIR3 | Corinth B | Zirje | Marine | 3 | 53.88 | 43.67 | 0.47 | 38.60 | 7.49 | 2.37 | 3.21 | 87.34 | 28.31 | 287.27 | 3.96 | 1.51 | 56095.20 | 8.90 | 193.02 |
| ZIR4 | Corinth B | Zirje | Marine | 2 | 25.63 | 42.53 | 0.47 | 35.85 | 7.29 | 2.44 | 3.42 | 83.36 | 22.63 | 263.32 | 2.80 | 1.47 | 44499.00 | 7.32 | 148.05 |
| ZIR5 | Corinth B | Zirje | Marine | 3 | 64.54 | 43.72 | 0.46 | 40.95 | 7.78 | 2.98 | 3.39 | 91.62 | 23.27 | 265.38 | 1.21 | 1.52 | 48418.10 | 9.07 | 139.69 |
| ZIR6 | Corinth B | Zirje | Marine | 3 | 22.86 | 40.82 | 0.43 | 32.80 | 6.93 | 2.75 | 2.98 | 80.96 | 19.36 | 252.21 | 4.99 | 1.34 | 39109.30 | 7.94 | 108.11 |
| ZIR7 | Corinth B | Zirje | Marine | 3 | 22.25 | 19.10 | 0.24 | 19.34 | 3.86 | 2.45 | 1.86 | 38.08 | 20.68 | 348.91 | 1.01 | 0.81 | 32802.90 | 2.66 | 172.42 |
| ZIR8 | Corinth B | Zirje | Marine | 2 | 30.29 | 19.11 | 0.30 | 17.86 | 3.81 | 2.62 | 1.86 | 37.69 | 20.38 | 349.38 | 0.85 | 0.82 | 33066.80 | 2.70 | 213.46 |
| ZIR9 | Corinth B | Zirje | Marine | 3 | 52.41 | 46.49 | 0.48 | 39.38 | 8.07 | 2.73 | 3.37 | 92.64 | 25.50 | 303.98 | 4.06 | 1.57 | 48906.40 | 7.99 | 201.05 |

| Table 1B: Continued geochemical composition of analysed amphorae measured by INAA |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample | Type | Site | Contx | FB | Rb | Sc | Sr | Ta | Tb | Th | Zn | Zr | Al | Ba | Ca | Dy | K | Mn | Na | Ti | V |
| CG1 | Corinth B | Crveni Grm | Terre. | 2 | 111.54 | 17.25 | 156.02 | 1.23 | 1.08 | 12.33 | 118.05 | 170.03 | 79141.0 | 315.2 | 73250.6 | 4.566 | 23652.9 | 1114.99 | 6638.3 | 4410.5 | 147.24 |
| CG2 | Corinth B | Crveni Grm | Terre. | 2 | 75.9 | 15.78 | 278.82 | 0.74 | 0.58 | 7.52 | 128.29 | 75.86 | 58283.4 | 341.2 | 105757 | 4.0838 | 17089.9 | 826.67 | 6972.1 | 3911.6 | 98.65 |
| CG3 | Corinth B | Crveni Grm | Terre. | 3 | 108.3 | 18.50 | 252.78 | 1.15 | 0.77 | 12.15 | 126.92 | 143.14 | 76673.1 | 382.6 | 70293.9 | 4.9098 | 20156 | 1144.96 | 6320 | 4512.6 | 132.92 |
| CG4 | Corinth B | Crveni Grm | Terre. | 4 | 112.93 | 22.03 | 240.56 | 1.27 | 0.82 | 15.57 | 172.47 | 116.73 | 102894.0 | 462.6 | 51366.4 | 5.8015 | 21600.3 | 1134.78 | 7504.4 | 5276.7 | 163.02 |
| CG5 | Corinth B | Crveni Grm | Terre. | 3 | 112.25 | 18.78 | 201.29 | 1.17 | 1.08 | 12.27 | 133.47 | 136.37 | 79625.6 | 343.9 | 69038 | 4.9891 | 20705.6 | 1100.77 | 6526.9 | 4665.6 | 119.94 |
| CG6 | Corinth B | Crveni Grm | Terre. | Unass. | 152.64 | 17.73 | 389.72 | 0.90 | 0.67 | 8.64 | 87.33 | 97.27 | 65087.7 | 337.4 | 105655.9 | 4.4515 | 14810.6 | 909.42 | 11926.6 | 3988.7 | 140.89 |
| GN1 | Corinth A' | Gnjilna | Marine | 5 | 63.52 | 18.10 | 1113.02 | 0.82 | 0.64 | 8.98 | 109.49 | 111.31 | 70887.4 | 200.3 | 105712.5 | 4.2241 | 14161.5 | 664.7 | 5765 | 3867.7 | 168.08 |
| GN2 | Corinth B | Gnjilna | Marine | 2 | 74.77 | 20.07 | 274.94 | 0.81 | 0.75 | 9.47 | 118.88 | 95.04 | 74737.6 | 235.2 | 67017.8 | 4.7836 | 17184.9 | 1172.65 | 9647.1 | 4186.5 | 143.2 |
| GN3 | Corinth B | Gnjilna | Marine | 2 | 87.54 | 19.27 | 181.91 | 0.97 | 0.57 | 9.72 | 103.48 | 122.4 | 80119.3 | 268.6 | 75453 | 3.7705 | 18806.8 | 757.26 | 7017.4 | 4305.7 | 116.38 |
| GN4 | Corinth B | Gnjilna | Marine | 2 | 52.38 | 15.25 | 1311.07 | 0.74 | 0.69 | 8.35 | 101.68 | 92.74 | 64765.1 | 145.3 | 129297.4 | 4.3144 | 12030.7 | 1347.19 | 5566.6 | 3548.6 | 121.8 |
| GN5 | Corinth B | Gnjilna | Marine | 2 | 43.03 | 16.19 | 507.28 | 0.72 | 0.73 | 8.74 | 107.97 | 107.27 | 68306.0 | 118.8 | 113505.9 | 4.7322 | 12717.5 | 2909.38 | 5460.7 | 3151.3 | 108.3 |
| GN6 | Corinth B | Gnjilna | Marine | 2 | 61.86 | 15.71 | 1002.51 | 0.75 | 0.67 | 8.52 | 103.84 | 102.25 | 65397.3 | 190.4 | 118089.2 | 4.0008 | 13660 | 1093.1 | 6707.3 | 3175.9 | 126.1 |
| GN7 | Corinth B | Gnjilna | Marine | 2 | 48.08 | 12.59 | 531.11 | 0.67 | 0.56 | 6.38 | 90.92 | 83.8 | 52106.2 | 187.1 | 141181.2 | 2.8952 | 12045.8 | 1109.51 | 6892.2 | 2403 | 94.71 |
| GN8 | Corinth B | Gnjilna | Marine | Unass. | 35.22 | 12.95 | 374.35 | 0.65 | 0.58 | 6.38 | 94.81 | 91.36 | 49028.0 | 171.4 | 121737 | 3.3209 | 13370.9 | 1712.59 | 6436.6 | 2958.1 | 116.88 |
| GN9 | Corinth B | Gnjilna | Marine | 2 | 24.81 | 12.48 | 507.87 | 0.72 | 0.59 | 6.23 | 88.45 | 81.27 | 53198.1 | 151.1 | 130322.6 | 3.2292 | 6799 | 711.36 | 7934.4 | 2503.1 | 75.29 |
| KOP1 | Corinth B | Kopila | Terre. | 4 | 72.88 | 23.38 | 88.66 | 1.34 | 1.24 | 15.40 | 162.04 | 148.06 | 110503.5 | 475.2 | 22608 | 6.5519 | 18605.6 | 1154.34 | 6480 | 6214.1 | 177.92 |
| KOP2 | Corinth B | Kopila | Terre. | 4 | 107.83 | 20.36 | 205.33 | 1.20 | 1.17 | 13.71 | 156.63 | 115.94 | 98607.3 | 506.7 | 48924.3 | 5.5053 | 22480.9 | 1119.41 | 9247.4 | 5155.5 | 145.82 |
| NAK1 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 121.44 | 13.65 | 450.38 | 1.03 | 0.89 | 9.94 | 130.99 | 96.5 | 71405.2 | 365.4 | 130623.2 | 4.0885 | 20297.7 | 812.99 | 5861.6 | 3425.7 | 88.98 |
| NAK10 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 106.08 | 12.48 | 316.67 | 1.04 | 0.79 | 9.69 | 112.47 | 96.07 | 62443.4 | 302.4 | 125439.3 | 3.8615 | 20058.9 | 748.74 | 6044.7 | 2946.4 | 79.91 |
| NAK15 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 74.45 | 15.71 | 508.44 | 1.27 | 0.88 | 11.03 | 159.01 | 93.24 | 79846.5 | 233.5 | 104268.8 | 4.1375 | 20554.7 | 1047.83 | 8511 | 3683.6 | 105.81 |
| NAK21 | Lamboglia 2 | Nak. Cave | Terre. | Unass. | 71.74 | 17.74 | 341.84 | 1.41 | 1.09 | 13.17 | 282.36 | 161.8 | 70606.9 | 368.4 | 90529.6 | 4.8925 | 18951.2 | 1500.82 | 3724.2 | 4421.3 | 72.65 |
| NAK24 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 286.06 | 12.44 | 494.92 | 0.99 | 0.65 | 9.94 | 109.33 | 139.07 | 62099.7 | 360 | 140452.4 | 3.9489 | 20196.4 | 748.65 | 5813.4 | 2937.2 | 93.73 |
| NAK26 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 214.11 | 13.13 | 541.8 | 1.05 | 0.80 | 9.27 | 177.29 | 106.75 | 63937.6 | 415.9 | 139682.6 | 4.1305 | 19292.5 | 820.26 | 7371.5 | 3538.4 | 83.02 |
| NAK27 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 132.89 | 14.74 | 370.91 | 1.13 | 0.60 | 10.31 | 164.37 | 99.73 | 72262.9 | 310 | 82164.7 | 4.4121 | 23254.8 | 1285.27 | 6968.2 | 3146.1 | 75.24 |
| NAK29 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 122.21 | 14.31 | 415.71 | 1.14 | 0.88 | 10.26 | 165.02 | 129.17 | 75011.0 | 465.4 | 101299.8 | 4.2208 | 24146.8 | 1004.37 | 6583.1 | 3569.3 | 107.44 |
| NAK3 | Lamboglia 2 | Nak. Cave | Terre. | Unass. | 108.95 | 16.26 | 385.03 | 0.80 | 0.56 | 7.79 | 110.4 | 92.8 | 65367.4 | 195.1 | 68971.5 | 3.6786 | 22994.7 | 747.53 | 8508.6 | 3451.7 | 100.81 |
| NAK30 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 124.91 | 14.40 | 382.67 | 1.16 | 0.67 | 11.28 | 193.78 | 101.82 | 74292.4 | 495.2 | 101488.5 | 4.8819 | 19694.3 | 967.76 | 7654.4 | 3680.5 | 87.54 |
| NAK31 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 108.87 | 15.49 | 549.98 | 1.28 | 0.69 | 11.96 | 144.08 | 129.12 | 74958.3 | 492.2 | 102481.9 | 4.8882 | 21201 | 1156.68 | 6762 | 3530.5 | 85.44 |
| NAK33 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 91.16 | 12.50 | 322.42 | 1.01 | 0.90 | 10.10 | 127.62 | 105.96 | 59254.9 | 428 | 123163.5 | 4.3338 | 20952.9 | 687.46 | 5986.3 | 2986.7 | 62.22 |
| NAK34 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 134.8 | 13.95 | 411.86 | 1.21 | 0.95 | 11.69 | 151.82 | 140.38 | 72324.2 | 486.3 | 79987.1 | 4.9957 | 25484.5 | 1259.56 | 8285.6 | 3917.1 | 99.26 |
| NAK4 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 134.76 | 14.74 | 413.42 | 1.17 | 0.71 | 10.04 | 144.01 | 104.21 | 75125.9 | 621.5 | 74630.2 | 4.1483 | 25237.4 | 768.63 | 6773.4 | 4456.6 | 88.27 |
| NAK5 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 125.93 | 13.49 | 426.91 | 1.04 | 0.79 | 9.50 | 233.04 | 108.14 | 73794.0 | 461.2 | 101195.6 | 3.9373 | 25203 | 841.81 | 6448.2 | 3485.7 | 86.27 |
| NAK6 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 130.39 | 14.83 | 412.79 | 1.19 | 0.78 | 11.25 | 178.67 | 123.72 | 75855.0 | 330.1 | 90088.7 | 4.6098 | 24983.9 | 964.33 | 6939.5 | 3696.7 | 103.82 |
| NAK7 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 78.54 | 11.84 | 370.7 | 0.99 | 0.79 | 8.92 | 132.71 | 103.25 | 55474.7 | 533.9 | 142315.2 | 4.162 | 19398.9 | 843.86 | 5578.6 | 2623.5 | 65.5 |
| NAK9 | Lamboglia 2 | Nak. Cave | Terre. | 1 | 125.82 | 14.63 | 450.15 | 1.19 | 0.87 | 10.49 | 147.16 | 109.51 | 77917.3 | 504.7 | 107639.8 | 4.5683 | 20803.1 | 1003.81 | 6788.7 | 3483.3 | 112.56 |
| POL1 | Lamboglia 2 | Polacisce | Marine | 1 | 108.06 | 12.94 | 405.38 | 1.15 | 0.70 | 10.16 | 96.76 | 100.67 | 69505.0 | 241.4 | 120931.2 | 3.9581 | 17980 | 692.63 | 9027.1 | 3739.1 | 101.01 |
| POL10 | Lamboglia 2 | Polacisce | Marine | Unass. | 101.68 | 17.92 | 178.03 | 0.95 | 0.80 | 12.04 | 114.93 | 131.83 | 83529.4 | 313.4 | 49713.7 | 4.0232 | 21504 | 603.36 | 8316.2 | 4149.6 | 141.85 |
| POL11 | Lamboglia 2 | Polacisce | Marine | 1 | 31.74 | 10.20 | 432.2 | 0.79 | 0.66 | 7.65 | 81.3 | 89.98 | 54706.0 | 132.6 | 109252.4 | 3.6478 | 10369.8 | 549.21 | 10148.5 | 2801.8 | 84.76 |
| POL12 | Lamboglia 2 | Polacisce | Marine | Unass. | 78.3 | 16.29 | 424.57 | 1.33 | 0.80 | 13.22 | 126.14 | 166.71 | 81450.5 | 323.8 | 72988.9 | 4.447 | 19535 | 744.16 | 12890.6 | 4574.5 | 153.07 |
| POL13 | Lamboglia 2 | Polacisce | Marine | Unass. | 77.29 | 14.42 | 315.79 | 1.13 | 0.81 | 10.95 | 117.62 | 131.48 | 71229.4 | 321.2 | 79830.6 | 4.1489 | 16233.6 | 506.78 | 9350.8 | 3850.3 | 131.23 |
| POL14 | Lamboglia 2 | Polacisce | Marine | 1 | 91.9 | 12.65 | 404.81 | 1.03 | 0.73 | 9.84 | 89.79 | 101.32 | 65675.1 | 243.4 | 128482.6 | 3.8332 | 17668.3 | 741.79 | 9030.5 | 3733.4 | 94.28 |
| POL15 | Lamboglia 2 | Polacisce | Marine | Unass. | 92.32 | 12.87 | 412.28 | 1.07 | 0.78 | 10.39 | 99.73 | 151.72 | 65712.5 | 265.4 | 116491.6 | 4.0288 | 15351.7 | 550.8 | 9799.7 | 3283.7 | 117.48 |
| POL16 | Lamboglia 2 | Polacisce | Marine | Unass. | 132.9 | 21.13 | 78.26 | 0.96 | 1.20 | 15.20 | 151.16 | 137.07 | 103809.8 | 462.7 | 34923.3 | 6.7604 | 24972.9 | 1242 | 10937 | 3599.8 | 153.37 |
| POL17 | Lamboglia 2 | Polacisce | Marine | 1 | 72.29 | 11.13 | 499.2 | 0.88 | 0.71 | 8.97 | 86.31 | 127.28 | 57725.8 | 305.4 | 135225.2 | 3.9646 | 14594.9 | 522.25 | 9578.3 | 3334.3 | 84.29 |
| POL18 | Lamboglia 2 | Polacisce | Marine | 1 | 99.92 | 12.78 | 428.82 | 0.97 | 0.65 | 9.10 | 95.34 | 109.54 | 69028.7 | 306.6 | 113470.9 | 3.42 | 20152.3 | 674.54 | 8565.5 | 2395 | 115.03 |
| POL19 | Lamboglia 2 | Polacisce | Marine | Unass. | 63.38 | 16.24 | 319.04 | 0.75 | 0.82 | 7.04 | 100.94 | 107.54 | 59806.1 | 129.1 | 92719.2 | 2.9723 | 13096.2 | 453.1 | 9073.6 | 3923.5 | 119.07 |
| POL19-1 | Lamboglia 2 | Polacisce | Marine | 1 | 84.3 | 12.94 | 683.94 | 0.97 | 0.61 | 8.85 | 98.7 | 75.51 | 63438.6 | 382.7 | 150314.3 | 3.3142 | 17510.8 | 950.06 | 10923.5 | 2901.2 | 106.08 |
| POL19-2 | Lamboglia 2 | Polacisce | Marine | 1 | 79.21 | 12.12 | 626.59 | 0.86 | 0.53 | 8.34 | 90.62 | 79.96 | 60306.0 | 287.5 | 170040.2 | 3.363 | 16330.7 | 948.15 | 10719.1 | 4081.5 | 101.43 |
| POL2 | Lamboglia 2 | Polacisce | Marine | Unass. | 46.46 | 12.95 | 471.59 | 1.70 | 1.27 | 11.92 | 81.71 | 190.19 | 71018.9 | 91.4 | 82428 | 5.9913 | 9303.9 | 472.06 | 5914.6 | 4498.5 | 113.65 |
| POL20 | Lamboglia 2 | Polacisce | Marine | Unass. | 80.89 | 13.14 | 388.8 | 1.34 | 0.77 | 10.57 | 89.45 | 188.6 | 78674.5 | 257.4 | 70375.3 | 4.4923 | 16006.8 | 441.69 | 3100.3 | 4333.1 | 124.01 |
| POL21 | Lamboglia 2 | Polacisce | Marine | 1 | 79.79 | 13.06 | 605.69 | 0.99 | 0.80 | 8.95 | 95.69 | 78.41 | 66269.4 | 235.8 | 130951.1 | 3.359 | 14302.7 | 1028.55 | 9188.6 | 2665.7 | 109.51 |
| POL22 | Lamboglia 2 | Polacisce | Marine | 1 | 75.15 | 11.36 | 602.85 | 0.92 | 0.70 | 9.27 | 85.78 | 132.72 | 58885.3 | 242.5 | 117503.7 | 3.9305 | 15472.2 | 575.4 | 10352.3 | 2582.8 | 76.99 |
| POL3 | Lamboglia 2 | Polacisce | Marine | 1 | 76.25 | 17.88 | 545.87 | 0.91 | 0.79 | 9.54 | 108.79 | 124.99 | 76818.8 | 298.8 | 76024.7 | 3.9145 | 18379.5 | 597.15 | 11138.2 | 4747.5 | 133.87 |
| POL4 | Lamboglia 2 | Polacisce | Marine | 1 | 92.26 | 12.66 | 555.69 | 1.01 | 0.68 | 9.51 | 97.89 | 80.65 | 83147.0 | 250.9 | 26046.5 | 5.0086 | 21516.3 | 511.05 | 10741.3 | 4650.6 | 123.71 |
| POL5 | Lamboglia 2 | Polacisce | Marine | 1 | 90.02 | 13.11 | 490.65 | 1.02 | 0.64 | 9.20 | 99.59 | 99.92 | 66177.5 | 166.8 | 124176.1 | 3.6286 | 17305.4 | 763.3 | 7967.8 | 2643 | 84.21 |
| POL6 | Lamboglia 2 | Polacisce | Marine | Unass. | 107.71 | 17.71 | 50.64 | 1.23 | 0.96 | 14.02 | 105.33 | 137.02 | 64032.1 | 354.3 | 132653.7 | 3.5787 | 15435.3 | 1031.01 | 8997.2 | 2783.1 | 119.41 |
| POL7 | Lamboglia 2 | Polacisce | Marine | 1 | 35.64 | 10.56 | 632.7 | 0.85 | 0.64 | 7.81 | 82.54 | 108.76 | 53672.2 | 189.7 | 122121.8 | 3.6052 | 10943.7 | 580.06 | 10671.9 | 2663.9 | 80.06 |
| POL8 | Lamboglia 2 | Polacisce | Marine | 1 | 109.96 | 13.44 | 442.14 | 1.06 | 0.77 | 9.51 | 100.36 | 73.35 | 67034.0 | 231.2 | 112119 | 3.9327 | 18390.5 | 832.87 | 9057.9 | 3783.2 | 93.67 |
| POL9 | Lamboglia 2 | Polacisce | Marine | 1 | 115.38 | 15.61 | 336.64 | 1.19 | 0.75 | 11.62 | 110.98 | 107.63 | 78586.0 | 327.3 | 79461 | 4.1785 | 20354.8 | 966.64 | 10167.2 | 3985.9 | 93.29 |
| RAT1 | Corinth B | Rat | Terre. | 2 | 75.27 | 12.94 | 533.77 | 1.08 | 0.82 | 10.95 | 96.73 | 121.89 | 87760.4 | 413.4 | 82094 | 3.9205 | 16859.3 | 679.68 | 14545.9 | 3730.9 | 88.55 |
| RAT2 | Corinth B | Rat | Terre. | 3 | 164.01 | 9.96 | 86.12 | 2.33 | 0.76 | 21.13 | 70.83 | 264.41 | 87324.4 | 383.1 | 4096.5 | 4.5588 | 19172 | 997.98 | 10341.2 | 3931.2 | 108.76 |
| RAT3 | Corinth B | Rat | Terre. | 3 | 93.63 | 17.60 | 407.33 | 0.84 | 0.63 | 8.68 | 109.15 | 98.61 | 70744.4 | 433.8 | 93030.3 | 4.2596 | 16747.1 | 942.53 | 10341 | 3914.8 | 113.05 |
| RAT4 | Corinth B | Rat | Terre. | 2 | 93.16 | 15.96 | 260.9 | 0.84 | 0.62 | 7.67 | 116.98 | 86.16 | 62281.7 | 387.8 | 87579.3 | 4.0404 | 17378.1 | 905.22 | 8188.6 | 3351.8 | 110.41 |
| RAT5 | Corinth B | Rat | Terre. | 2 | 99.07 | 14.60 | 311.64 | 0.72 | 0.53 | 7.05 | 108.56 | 99.48 | 61137.7 | 325.2 | 102958.5 | 3.7495 | 22027.4 | 817.85 | 8079.6 | 3489 | 97.1 |
| RAT6 | Corinth B | Rat | Terre. | 2 | 96.91 | 18.37 | 278.53 | 1.01 | 0.85 | 10.12 | 112.81 | 110.21 | 75062.9 | 504.5 | 77471.1 | 4.4572 | 18194.3 | 1121.3 | 9786.9 | 4230.9 | 136.21 |
| RAT7 | Corinth B | Rat | Terre. | 2 | 93.55 | 15.06 | 320.66 | 0.79 | 0.79 | 7.55 | 104.6 | 82.23 | 61472.8 | 407.6 | 97034.5 | 3.7935 | 17814.8 | 984.41 | 8992.2 | 3910.2 | 89.41 |
| RAT8 | Corinth B | Rat | Terre. | 4 | 119.95 | 20.69 | 235.28 | 1.21 | 1.16 | 13.87 | 149.52 | 114.95 | 102566.4 | 534.9 | 57362.6 | 5.4068 | 22189.5 | 1094.72 | 9287.8 | 5719.1 | 141.36 |
| RES1 | Lamboglia 2 | Resnik | Terre. | 1 | 75.83 | 14.18 | 492.71 | 1.04 | 0.80 | 10.38 | 83.77 | 84.98 | 71909.8 | 513.3 | 124766.4 | 4.1639 | 14566.9 | 842.23 | 7097.5 | 3631.1 | 94.09 |
| RES10 | Lamboglia 2 | Resnik | Terre. | 1 | 85.74 | 14.24 | 358.47 | 1.15 | 0.89 | 11.05 | 103.02 | 87.57 | 74869.6 | 662 | 100430.2 | 4.8567 | 16455.6 | 1429.37 | 4442.8 | 4648.4 | 77.99 |
| RES11 | Lamboglia 2 | Resnik | Terre. | Unass. | 49.65 | 13.90 | 594.91 | 1.05 | 0.93 | 11.05 | 76.01 | 133.41 | 63290.7 | 645 | 137135.2 | 4.6535 | 12142.1 | 942.17 | 6166.2 | 3841.9 | 78.97 |
| RES12 | Lamboglia 2 | Resnik | Terre. | 1 | 107.64 | 14.39 | 394.1 | 1.11 | 0.93 | 10.44 | 102.55 | 97.2 | 72947.5 | 633.4 | 86806.4 | 4.1376 | 20462.8 | 1179.98 | 6400.4 | 4539.3 | 99.97 |
| RES13 | Lamboglia 2 | Resnik | Terre. | 1 | 104.83 | 13.73 | 285.89 | 1.00 | 1.06 | 11.04 | 95.01 | 115.52 | 68818.3 | 550.9 | 84234.4 | 4.9079 | 16229.3 | 818.47 | 4853.3 | 4351.5 | 97.6 |
| RES14 | Lamboglia 2 | Resnik | Terre. | 1 | 109.44 | 14.37 | 394.4 | 1.13 | 1.06 | 10.25 | 95.16 | 114.94 | 73314.5 | 405 | 101809.1 | 4.2125 | 18252.4 | 1023.22 | 7086.3 | 3908.2 | 112.79 |
| RES15 | Lamboglia 2 | Resnik | Terre. | 1 | 82.33 | 13.12 | 244.56 | 1.10 | 0.90 | 10.63 | 102.29 | 107.46 | 70229.3 | 506.2 | 105427.9 | 4.3538 | 17446.2 | 922.18 | 4499.5 | 3725.6 | 76.33 |
| RES16 | Lamboglia 2 | Resnik | Terre. | Unass. | 79.18 | 11.80 | 430.58 | 0.96 | 0.83 | 9.29 | 103.24 | 90.13 | 56378.9 | 701.6 | 146934.8 | 3.692 | 13468.2 | 1026.84 | 3772.8 | 3198.5 | 62.2 |
| RES17 | Lamboglia 2 | Resnik | Terre. | 1 | 60.83 | 12.22 | 417.12 | 0.96 | 0.78 | 9.64 | 71.14 | 118.36 | 57815.7 | 583.3 | 122838.2 | 3.9948 | 10636.7 | 795.73 | 5084.1 | 3239.4 | 79.38 |
| RES18 | Lamboglia 2 | Resnik | Terre. | Unass. | 59.5 | 16.67 | 251.71 | 0.79 | 0.97 | 8.93 | 99.32 | 82.42 | 67906.2 | 739.1 | 118424.3 | 4.1886 | 15855.7 | 1601.94 | 3856.5 | 3799.7 | 81.01 |
| RES19 | Lamboglia 2 | Resnik | Terre. | 1 | 59.26 | 12.82 | 400.9 | 1.01 | 0.75 | 9.40 | 104.45 | 98.1 | 68651.9 | 429 | 133016.1 | 4.156 | 12166.7 | 901.02 | 3364.2 | 3434.7 | 76.59 |
| RES2 | Lamboglia 2 | Resnik | Terre. | 1 | 93.14 | 14.39 | 316.56 | 1.14 | 0.82 | 11.09 | 106.96 | 103.98 | 78774.0 | 531 | 91429.3 | 4.2673 | 18165.5 | 943.8 | 6381.4 | 3866.7 | 89.26 |
| RES20 | Lamboglia 2 | Resnik | Terre. | 1 | 83.26 | 15.83 | 328.78 | 1.23 | 0.92 | 11.40 | 102.55 | 116.49 | 80180.7 | 421.6 | 75087.5 | 4.6682 | 19722.5 | 1138.29 | 6136.1 | 4542.1 | 98.27 |
| RES21 | Lamboglia 2 | Resnik | Terre. | Unass. | 75.04 | 14.93 | 484.91 | 1.16 | 0.81 | 10.46 | 96.8 | 82.81 | 79327.9 | 565.2 | 113426.6 | 4.2433 | 16702.1 | 895.69 | 3284.6 | 3801.9 | 109.12 |
| RES22 | Lamboglia 2 | Resnik | Terre. | 1 | 101.93 | 13.85 | 297.52 | 1.15 | 0.92 | 11.55 | 101.44 | 121.14 | 79608.4 | 507.3 | 79947.2 | 4.5855 | 16989.4 | 970.57 | 6603.9 | 3683.3 | 98.39 |
| RES23 | Lamboglia 2 | Resnik | Terre. | 1 | 101.65 | 14.18 | 161.85 | 1.21 | 0.92 | 12.01 | 103.88 | 111.26 | 74131.9 | 594.2 | 71083.9 | 5.0348 | 22798.4 | 995.96 | 7712 | 4238.6 | 87.17 |
| RES24 | Lamboglia 2 | Resnik | Terre. | 1 | 107.25 | 12.41 | 239.87 | 1.05 | 0.95 | 10.63 | 92.55 | 84.1 | 67531.1 | 551.1 | 93049.1 | 4.347 | 18519.7 | 755.19 | 7343 | 3985.2 | 95.48 |
| RES25 | Lamboglia 2 | Resnik | Terre. | 1 | 128.41 | 16.63 | 520.5 | 1.18 | 1.07 | 12.03 | 95.78 | 106.18 | 82486.8 | 820.3 | 86029.8 | 4.9062 | 25591.7 | 1354.13 | 4314.7 | 4049.9 | 122.51 |
| RES26 | Lamboglia 2 | Resnik | Terre. | Unass. | 61.86 | 11.47 | 463.12 | 0.93 | 0.72 | 8.88 | 88.2 | 84.93 | 62029.4 | 650.9 | 141127.3 | 4.2544 | 10656.4 | 1352.97 | 4080.3 | 3415.9 | 60.37 |
| RES27 | Lamboglia 2 | Resnik | Terre. | 1 | 91.77 | 15.33 | 384.02 | 1.23 | 1.12 | 12.35 | 103.61 | 121.47 | 84006.3 | 347.9 | 70022.4 | 4.8283 | 19911 | 752.68 | 8299.6 | 4338.2 | 101.57 |
| RES28 | Lamboglia 2 | Resnik | Terre. | 1 | 53.48 | 12.89 | 496.31 | 1.04 | 0.92 | 9.01 | 83.02 | 92.06 | 70323.9 | 648.2 | 140654.6 | 4.0907 | 12002.7 | 1127.05 | 3009.9 | 3582.4 | 88.11 |
| RES29 | Lamboglia 2 | Resnik | Terre. | Unass. | 94.05 | 14.50 | 318.12 | 1.13 | 1.02 | 10.85 | 98.16 | 73.07 | 74132.7 | 497.3 | 97001.5 | 4.7006 | 20036.8 | 1010.13 | 6624.7 | 4315.5 | 83.74 |
| RES3 | Lamboglia 2 | Resnik | Terre. | 1 | 98.34 | 12.72 | 259.88 | 1.04 | 0.85 | 10.92 | 85.6 | 117.07 | 64895.2 | 691.6 | 93028 | 4.4006 | 19713.8 | 727.96 | 6750.5 | 3247.7 | 99.01 |
| RES30 | Lamboglia 2 | Resnik | Terre. | 1 | 90.25 | 15.30 | 303.67 | 1.25 | 0.95 | 11.84 | 104.67 | 103.59 | 80742.1 | 507.2 | 84164.5 | 5.0417 | 18428.6 | 1023.43 | 6469.4 | 4023.8 | 85.43 |
| RES31 | Lamboglia 2 | Resnik | Terre. | Unass. | 88.24 | 15.22 | 287.15 | 1.30 | 1.09 | 11.91 | 110.12 | 108.24 | 100300.6 | 528.4 | 105786 | 5.6386 | 23503.6 | 1662.3 | 6398.6 | 5371 | 119.1 |
| RES32 | Lamboglia 2 | Resnik | Terre. | 1 | 84.33 | 15.70 | 324.34 | 1.16 | 1.12 | 11.11 | 107.77 | 115.95 | 81704.4 | 384.1 | 83950.8 | 4.435 | 15285 | 1323.59 | 5079.7 | 3871.1 | 101.17 |
| RES33 | Lamboglia 2 | Resnik | Terre. | 1 | 65.88 | 12.93 | 471.86 | 1.01 | 0.73 | 9.24 | 86.68 | 75.59 | 67693.3 | 479.1 | 150204.9 | 4.0251 | 12799.8 | 843.44 | 3433.6 | 3247.4 | 92.67 |
| RES34 | Lamboglia 2 | Resnik | Terre. | Unass. | 94.82 | 16.14 | 459.63 | 1.25 | 0.83 | 12.31 | 102.6 | 101.88 | 92823.5 | 530.3 | 94066.4 | 4.7303 | 21480.5 | 1443.48 | 5621.6 | 4232 | 108.22 |
| RES35 | Lamboglia 2 | Resnik | Terre. | 1 | 115.9 | 13.16 | 246.78 | 1.26 | 1.02 | 11.74 | 123.27 | 114.83 | 84575.2 | 524.4 | 80187.3 | 4.9983 | 21092 | 786.17 | 8040.9 | 4128.6 | 86.58 |
| RES4 | Lamboglia 2 | Resnik | Terre. | 1 | 59.15 | 13.72 | 419.4 | 1.16 | 0.83 | 10.26 | 98.42 | 93.92 | 69205.0 | 704.4 | 123133 | 4.2042 | 15909.5 | 885.15 | 3050.6 | 3688.6 | 59.32 |
| RES5 | Lamboglia 2 | Resnik | Terre. | Unass. | 106.76 | 13.61 | 367.47 | 1.14 | 1.19 | 11.47 | 91.42 | 118.91 | 68803.6 | 682.6 | 87010.5 | 4.5825 | 20784.7 | 906.09 | 6506.9 | 3719.4 | 75.17 |
| RES6 | Lamboglia 2 | Resnik | Terre. | Unass. | 100.4 | 14.97 | 371.73 | 1.17 | 1.00 | 10.66 | 102.27 | 88.41 | 75670.7 | 512 | 92397 | 4.0291 | 18434.6 | 985.74 | 5872.3 | 3983.9 | 89.87 |
| RES7 | Lamboglia 2 | Resnik | Terre. | Unass. | 76.66 | 19.67 | 197.54 | 1.03 | 0.64 | 9.18 | 115.3 | 98.12 | 72082.3 | 299.1 | 82285.4 | 3.8964 | 16503.9 | 821.74 | 6909.3 | 4100 | 94.33 |
| RES8 | Lamboglia 2 | Resnik | Terre. | Unass. | 73.76 | 15.02 | 308.22 | 1.22 | 0.90 | 11.79 | 101.24 | 104.79 | 73385.6 | 531.9 | 97040.3 | 4.8068 | 17589.5 | 960.28 | 10139.1 | 3538.6 | 123.9 |
| RES9 | Lamboglia 2 | Resnik | Terre. | Unass. | 93.34 | 13.65 | 316.77 | 0.97 | 0.79 | 10.89 | 99.17 | 136.65 | 67318.0 | 612.8 | 90915.7 | 4.5569 | 15442 | 827.46 | 4015.8 | 4017 | 84.18 |
| SC1 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 73.86 | 10.71 | 596.44 | 0.92 | 0.68 | 8.17 | 133.3 | 112.07 | 58877.7 | 305.6 | 114363.4 | 3.6843 | 14649.9 | 722.38 | 4316.6 | 3193.4 | 85.33 |
| SC10 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 44.9 | 9.26 | 376.26 | 1.11 | 0.70 | 8.26 | 79.06 | 193.22 | 57766.6 | 202.9 | 98873.6 | 3.7715 | 13517.5 | 479.67 | 7812.5 | 3317.7 | 90.61 |
| SC11 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 82.86 | 12.18 | 750.91 | 1.36 | 0.80 | 9.65 | 86.81 | 159.67 | 69812.0 | 196.8 | 71889.7 | 4.156 | 17569.5 | 327.74 | 5429.9 | 4285.1 | 105.74 |
| SC12 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 78.29 | 18.16 | 241.72 | 1.03 | 0.84 | 10.02 | 123.06 | 118.98 | 78520.2 | 220.6 | 73053.3 | 5.028 | 17084.1 | 715.43 | 12404.5 | 4134.7 | 107.54 |
| SC13 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 78.87 | 11.67 | 330.15 | 1.26 | 0.88 | 10.03 | 83.99 | 214.05 | 70030.8 | 280.1 | 50522.7 | 4.0857 | 20389.7 | 247.75 | 5951.5 | 4544.1 | 95.61 |
| SC2 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 81.45 | 10.97 | 709.85 | 0.86 | 0.64 | 8.48 | 88 | 127.36 | 65846.1 | 3440.9 | 115844.4 | 3.7555 | 15229.1 | 709.46 | 4674.1 | 2891 | 101.16 |
| SC3 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 68.54 | 12.13 | 735.03 | 1.05 | 0.68 | 9.32 | 88.79 | 146.81 | 68608.6 | 340.8 | 86890.9 | 3.8877 | 13135.7 | 749.6 | 5603.5 | 3020.2 | 120.93 |
| SC4 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 23.91 | 12.07 | 1017.83 | 1.02 | 0.74 | 9.17 | 189.04 | 116.68 | 65782.4 | 372.2 | 137033 | 4.0158 | 3222.2 | 808.39 | 11660.7 | 3371.3 | 105.74 |
| SC5 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 70.9 | 11.52 | 649.19 | 0.98 | 0.70 | 8.52 | 137.66 | 97.27 | 63253.6 | 394.6 | 112778.2 | 3.8397 | 14700.3 | 1024.91 | 5659.3 | 3297.8 | 103.96 |
| SC6 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 98.21 | 13.76 | 383.07 | 1.52 | 0.84 | 10.99 | 100.89 | 193.72 | 80989.4 | 175.6 | 32571.7 | 4.6092 | 21634.8 | 294.04 | 5076.4 | 4677.3 | 118.45 |
| SC7 | Lamboglia 2 | Supetar - Cavtat | Marine | 1 | 48.86 | 9.79 | 487.77 | 1.06 | 0.68 | 7.61 | 69.87 | 165.09 | 55501.4 | 197.3 | 114938.6 | 3.2515 | 12960.5 | 533.75 | 5767.8 | 3258.3 | 75.74 |
| SC8 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 93.84 | 13.75 | 277.41 | 1.53 | 0.87 | 11.03 | 99.35 | 182.05 | 80598.9 | 303.4 | 33734 | 4.598 | 22536.5 | 370.49 | 7017.8 | 4416.2 | 127 |
| SC9 | Lamboglia 2 | Supetar - Cavtat | Marine | Unass. | 89.19 | 12.71 | 296.14 | 1.42 | 0.88 | 10.93 | 92.82 | 204.46 | 75427.0 | 253.2 | 30361.9 | 4.4736 | 20643.3 | 248.51 | 5965 | 3898.3 | 102.38 |
| SGP1 | Greco-Italic | Pharos | Terre. | 2 | 106.06 | 13.83 | 254.47 | 0.94 | 0.85 | 10.26 | 139.4 | 105.83 | 71444.0 | 384.6 | 132923.2 | 4.2244 | 10150.2 | 987.46 | 10849.3 | 3676.5 | 79.2 |
| SGP10 | Corinth B | Pharos | Terre. | 2 | 96.31 | 15.15 | 348.82 | 0.71 | 0.72 | 7.21 | 105.55 | 92.06 | 55633.8 | 397.5 | 113835 | 3.7045 | 18088.8 | 1029.54 | 6402.6 | 2809.8 | 83.9 |
| SGP11 | Corinth B | Pharos | Terre. | 2 | 119.76 | 16.08 | 389.26 | 0.79 | 1.02 | 7.84 | 83.6 | 117.69 | 64122.9 | 423.4 | 96823.6 | 4.5562 | 18748 | 1130.8 | 10212 | 3339.2 | 116.46 |
| SGP12 | Hellenistic | Pharos | Terre. | 4 | 130.44 | 19.79 | 177.32 | 1.18 | 1.38 | 13.59 | 147.76 | 107.33 | 93500.7 | 439.9 | 42768.9 | 5.6013 | 26566 | 1053.95 | 9486.8 | 5127.7 | 153.32 |
| SGP13 | Hellenistic | Pharos | Terre. | 2 | 105.89 | 16.30 | 322.85 | 0.73 | 0.92 | 7.82 | 97.25 | 92.64 | 61196.4 | 336.5 | 85989.8 | 4.0263 | 19016.4 | 1170.11 | 8132.4 | 3365.8 | 107.35 |
| SGP14 | Hellenistic | Pharos | Terre. | 2 | 146.36 | 16.11 | 171.16 | 1.37 | 1.04 | 13.62 | 122.37 | 139.63 | 82373.1 | 513.6 | 38525.8 | 5.4323 | 24510 | 853.32 | 9263.7 | 4227.2 | 133.11 |
| SGP15 | Hellenistic | Pharos | Terre. | 6 | 139.94 | 16.84 | 381.73 | 1.29 | 1.02 | 12.99 | 101.82 | 118.24 | 81688.1 | 466.9 | 77496.2 | 5.7677 | 21176.8 | 1024.83 | 8232 | 3903.5 | 135.94 |
| SGP16 | Hellenistic | Pharos | Terre. | 6 | 129.59 | 17.19 | 390.72 | 1.26 | 1.21 | 13.78 | 106.09 | 171.99 | 80045.0 | 479.4 | 72498.5 | 5.7636 | 23462.1 | 976.21 | 8819.1 | 4389.8 | 138.26 |
| SGP17 | Corinth A' | Pharos | Terre. | 5 | 135.21 | 20.24 | 450.08 | 0.80 | 0.69 | 9.64 | 115.45 | 98.07 | 80520.9 | 444.6 | 109868.4 | 4.0075 | 24924.3 | 1221.8 | 3609 | 3977.3 | 152.94 |
| SGP18 | Greco-Italic | Pharos | Terre. | 2 | 132.37 | 15.57 | 584.96 | 1.09 | 0.94 | 10.73 | 107.09 | 110.63 | 80884.6 | 515.2 | 114081.6 | 4.1559 | 21989.9 | 1514.54 | 5130 | 3296.3 | 113.41 |
| SGP19 | Corinth B | Pharos | Terre. | 3 | 146.3 | 15.64 | 191.77 | 1.53 | 1.27 | 15.91 | 105.38 | 203.44 | 82107.2 | 513 | 38286.4 | 5.9536 | 23595.8 | 717.93 | 9651.6 | 4488.4 | 106.28 |
| SGP2 | Corinth B | Pharos | Terre. | 2 | 106.08 | 16.10 | 393.2 | 0.76 | 0.94 | 7.86 | 118.34 | 108.04 | 63346.6 | 335.7 | 95598.9 | 3.9629 | 21823.4 | 1028.57 | 9656.1 | 3626.2 | 110.22 |
| SGP20 | Hellenistic | Pharos | Terre. | 7 | 132.86 | 20.05 | 298.28 | 1.32 | 1.14 | 15.92 | 120.93 | 148.29 | 89993.7 | 467.2 | 69186.1 | 5.8116 | 21139.5 | 1593.59 | 5572.4 | 4559.4 | 168.17 |
| SGP21 | Corinth B | Pharos | Terre. | 3 | 130.97 | 18.09 | 169.86 | 1.47 | 1.15 | 15.84 | 121.57 | 151.99 | 88565.6 | 451.7 | 30337.8 | 6.2545 | 21324.9 | 1129.79 | 5087.8 | 5043 | 157.42 |
| SGP22 | Hellenistic | Pharos | Terre. | 6 | 128.27 | 14.36 | 168.52 | 1.34 | 1.03 | 14.51 | 97.05 | 144.4 | 82042.3 | 416.5 | 54829.8 | 4.9856 | 20639.3 | 634.75 | 8904.4 | 4129 | 118.54 |
| SGP23 | Greco-Italic | Pharos | Terre. | 2 | 83.51 | 10.77 | 433.28 | 0.84 | 0.86 | 8.26 | 100.53 | 90.85 | 52125.6 | 379.8 | 159901.8 | 3.6172 | 16015.7 | 983.69 | 5345.8 | 2709.5 | 73.87 |
| SGP24 | Hellenistic | Pharos | Terre. | 2 | 110.53 | 13.38 | 442.72 | 1.15 | 0.80 | 10.95 | 95.96 | 90.94 | 74424.6 | 581.5 | 79154.7 | 4.201 | 24352.8 | 840.32 | 9832.9 | 4386.9 | 103.13 |
| SGP25 | Hellenistic | Pharos | Terre. | 4 | 132.69 | 21.58 | 285.64 | 1.34 | 1.12 | 15.47 | 157.07 | 100.18 | 101570.6 | 553.7 | 55907.3 | 5.7824 | 24616.6 | 1067.45 | 8278.4 | 5072.8 | 165.18 |
| SGP26 | Hellenistic | Pharos | Terre. | Unass. | 95.85 | 14.24 | 106.93 | 1.16 | 0.92 | 11.47 | 114.15 | 147.76 | 68974.1 | 329.1 | 73911.6 | 5.3527 | 11532.6 | 881.47 | 3441.8 | 4767.5 | 143.95 |
| SGP27 | Lamboglia 2 | Pharos | Terre. | 1 | 105.53 | 12.37 | 250.78 | 1.02 | 0.71 | 10.32 | 101.94 | 100.19 | 64846.8 | 404.8 | 91118.3 | 4.0234 | 22277.9 | 676.51 | 6656.1 | 3443 | 87.44 |
| SGP3 | Corinth B | Pharos | Terre. | 2 | 89.18 | 13.35 | 249.08 | 0.70 | 0.71 | 9.47 | 81.37 | 99.43 | 59258.6 | 337.7 | 124604.6 | 3.5325 | 17953.1 | 1142.66 | 2391.7 | 2622.4 | 97.44 |
| SGP4 | Corinth B | Pharos | Terre. | 2 | 91.29 | 19.49 | 364.64 | 0.74 | 0.95 | 7.51 | 97.91 | 102.31 | 69888.4 | 343 | 88163.1 | 3.8257 | 15921 | 1033.33 | 8067.7 | 4638.5 | 114.54 |
| SGP5 | Corinth B | Pharos | Terre. | 2 | 109.07 | 15.30 | 318.8 | 0.79 | 0.64 | 7.31 | 95.99 | 122.16 | 56171.9 | 373 | 98970.5 | 3.7588 | 20510.1 | 971.03 | 7701.1 | 3111.4 | 99.24 |
| SGP6 | Corinth B | Pharos | Terre. | 3 | 123.85 | 17.73 | 113.72 | 1.26 | 1.06 | 15.29 | 124.8 | 200.49 | 86554.0 | 400.7 | 34990 | 5.9349 | 19389.3 | 1172.1 | 5312.5 | 4378.7 | 156.71 |
| SGP7 | Hellenistic | Pharos | Terre. | 7 | 160.4 | 19.31 | 53 | 1.90 | 1.36 | 24.64 | 151.31 | 267.97 | 115743.4 | 407.8 | 9496.3 | 7.8748 | 18056.8 | 1267.4 | 3381 | 5605.5 | 207.58 |
| SGP8 | Hellenistic | Pharos | Terre. | 4 | 133.87 | 20.93 | 231.32 | 1.23 | 1.27 | 14.48 | 152.19 | 115.53 | 103391.7 | 483.6 | 55821.8 | 6.0995 | 24770.5 | 1169.59 | 10566.3 | 5063.3 | 150.12 |
| SGP9 | Corinth B | Pharos | Terre. | 2 | 107.02 | 16.17 | 407.11 | 0.72 | 0.59 | 7.94 | 123.04 | 105.77 | 63932.5 | 358.7 | 102320.2 | 3.9961 | 20115.3 | 941.57 | 7684.2 | 3470.7 | 119.74 |
| SOK1 | Corinth B | Sokol | Terre. | Unass. | 141.32 | 13.44 | 364.24 | 1.25 | 0.91 | 12.64 | 90.14 | 128.84 | 74714.4 | 500.3 | 119861.7 | 4.1708 | 15862.1 | 726.97 | 9902.5 | 3824.8 | 115.3 |
| SOK10 | Corinth B | Sokol | Terre. | 2 | 71.83 | 19.52 | 316.99 | 1.05 | 0.70 | 10.84 | 148.24 | 121.21 | 77827.1 | 570.9 | 71205.9 | 4.7443 | 16727.4 | 1059.05 | 8269.6 | 4290.3 | 110.24 |
| SOK11 | Corinth B | Sokol | Terre. | 2 | 52.48 | 18.87 | 340.19 | 0.86 | 0.66 | 8.89 | 142.83 | 125.86 | 71509.6 | 692.7 | 92848.3 | 4.5191 | 14904.2 | 980.61 | 4769.7 | 4248.2 | 107.96 |
| SOK12 | Hellenistic | Sokol | Terre. | 2 | 51.24 | 18.57 | 396.65 | 0.87 | 0.75 | 9.97 | 134.96 | 95.31 | 70219.4 | 462.9 | 99869.2 | 4.0569 | 13805.9 | 1036.58 | 9715.7 | 3911.2 | 88.2 |
| SOK13 | Corinth B | Sokol | Terre. | 2 | 92.38 | 17.98 | 128.58 | 0.92 | 0.67 | 10.14 | 156.1 | 97.08 | 70225.0 | 659 | 57689.8 | 4.3827 | 20758.4 | 957.24 | 8870.9 | 3803.5 | 101.32 |
| SOK14 | Hellenistic | Sokol | Terre. | 2 | 55.19 | 17.00 | 235.75 | 0.84 | 0.67 | 8.58 | 140.64 | 129.51 | 67697.5 | 563.4 | 81147.2 | 4.0849 | 13352.6 | 896.41 | 6871.8 | 3616.1 | 94.77 |
| SOK15 | Hellenistic | Sokol | Terre. | 2 | 90.43 | 16.88 | 171.2 | 1.31 | 1.09 | 13.59 | 134.42 | 127.85 | 82279.0 | 647.7 | 60836.8 | 5.4877 | 20441.8 | 1039.3 | 7095.4 | 4127.8 | 69.21 |
| SOK2 | Corinth B | Sokol | Terre. | 6 | 84.35 | 17.25 | 442.63 | 1.28 | 0.78 | 12.22 | 128.5 | 122.52 | 85320.3 | 568.7 | 90506.6 | 4.8279 | 19955.5 | 1171.6 | 4948.1 | 3981.9 | 103.16 |
| SOK3 | Corinth B | Sokol | Terre. | 2 | 56.45 | 18.98 | 305.19 | 0.85 | 0.72 | 8.99 | 149.16 | 89.78 | 77202.7 | 712.6 | 92934.8 | 4.869 | 14649.2 | 970.26 | 4914.7 | 4336.8 | 109.89 |
| SOK4 | Corinth B | Sokol | Terre. | Unass. | 54.24 | 17.20 | 0 | 0.84 | 0.68 | 8.64 | 167.17 | 102.88 | 70884.2 | 543.5 | 87839.6 | 4.2294 | 15082.7 | 835.62 | 7122.9 | 4200.9 | 90.79 |
| SOK5 | Corinth B | Sokol | Terre. | 2 | 48.83 | 19.27 | 208.19 | 0.88 | 0.72 | 9.06 | 166.34 | 104.79 | 81073.3 | 604.9 | 67513.5 | 4.6024 | 14366.3 | 1207.56 | 5918.6 | 4104.2 | 101.64 |
| SOK6 | Greco-Italic | Sokol | Terre. | 2 | 78.14 | 12.53 | 336.74 | 0.97 | 0.83 | 9.05 | 97.86 | 111.41 | 66202.9 | 511.8 | 137727.1 | 4.0726 | 18275.8 | 790.61 | 3116.2 | 2824 | 80 |
| SOK7 | Corinth B | Sokol | Terre. | 2 | 106.34 | 17.28 | 293.68 | 0.79 | 0.67 | 8.30 | 116.15 | 102.04 | 65064.9 | 477.8 | 83551.6 | 4.1148 | 20490.1 | 858.94 | 8815.1 | 3242.9 | 103.43 |
| SOK8 | Hellenistic | Sokol | Terre. | 6 | 77.05 | 18.21 | 410.37 | 1.43 | 0.94 | 14.18 | 120.62 | 150.08 | 88363.9 | 507.6 | 77845.2 | 6.0043 | 19347.5 | 1188.82 | 7050.7 | 3808.5 | 128.69 |
| SOK9 | Corinth B | Sokol | Terre. | 2 | 61.93 | 17.11 | 318.05 | 0.81 | 0.74 | 8.36 | 106.06 | 85.21 | 67099.1 | 465.9 | 91379 | 4.4915 | 15064.5 | 916.57 | 7565.8 | 3508.1 | 112.57 |
| STI1 | Corinth B | Stine | Terre. | 3 | 94.97 | 18.85 | 66.25 | 1.61 | 1.29 | 20.77 | 137.65 | 233.73 | 89339.9 | 311.6 | 28082.9 | 7.7277 | 14599.9 | 1275.03 | 4224.7 | 5507.7 | 130.04 |
| STI2 | Corinth B | Stine | Terre. | 3 | 109.27 | 16.75 | 96.93 | 1.52 | 1.38 | 17.62 | 130.11 | 271.96 | 79507.3 | 375.3 | 19596.3 | 6.6929 | 15585.3 | 1150.3 | 5695.4 | 5153 | 107.6 |
| VIC1 | Corinth B | Vilina Cave | Terre. | 4 | 131.55 | 20.27 | 239.86 | 1.29 | 0.87 | 13.94 | 163.63 | 125.51 | 103121.6 | 609.4 | 52982.3 | 5.3921 | 24704.8 | 1091.24 | 9303.1 | 4369 | 141.06 |
| VIC10 | Corinth B | Vilina Cave | Terre. | 2 | 113.52 | 16.68 | 345.67 | 0.84 | 0.86 | 8.24 | 141.38 | 117.96 | 67418.5 | 324.6 | 88189.5 | 4.0924 | 21419.6 | 900.32 | 10966 | 3734.3 | 121.07 |
| VIC11 | Corinth B | Vilina Cave | Terre. | 2 | 108.43 | 16.78 | 266.41 | 0.81 | 0.82 | 8.08 | 178.62 | 96.89 | 70245.1 | 302.5 | 59322 | 3.4445 | 21382.3 | 708.5 | 7759.3 | 3707.4 | 102.96 |
| VIC12 | Corinth B | Vilina Cave | Terre. | 2 | 111.68 | 16.89 | 263.91 | 0.79 | 0.90 | 8.23 | 170.85 | 97.32 | 65868.5 | 350 | 77767.1 | 4.1755 | 21547.2 | 811.8 | 8796.6 | 4278.3 | 120.26 |
| VIC13 | Corinth B | Vilina Cave | Terre. | 2 | 113 | 16.18 | 276.87 | 0.69 | 0.61 | 7.82 | 132.83 | 88.79 | 64985.5 | 296.7 | 79520.1 | 3.8161 | 24929.9 | 838.51 | 8904.7 | 4367.8 | 113.9 |
| VIC14 | Corinth B | Vilina Cave | Terre. | 2 | 109.21 | 17.13 | 257.4 | 0.79 | 0.76 | 8.17 | 247.58 | 96.85 | 70765.3 | 351.5 | 80250.1 | 4.2431 | 21002.6 | 847.06 | 8684.3 | 3485.5 | 110.31 |
| VIC15 | Corinth B | Vilina Cave | Terre. | 2 | 78.42 | 17.29 | 137.03 | 0.83 | 0.80 | 8.96 | 186.86 | 110.03 | 71451.4 | 344.8 | 50632.3 | 4.7737 | 17153.8 | 975.56 | 8343.7 | 4590.3 | 99.65 |
| VIC16 | Corinth B | Vilina Cave | Terre. | 2 | 104.9 | 15.15 | 276.15 | 0.72 | 0.77 | 7.56 | 197.09 | 84.02 | 61926.6 | 292 | 88315.4 | 3.5697 | 18655 | 801.06 | 9515.9 | 3253.2 | 111.07 |
| VIC17 | Corinth B | Vilina Cave | Terre. | Unass. | 111.86 | 17.10 | 296.04 | 0.84 | 0.67 | 8.27 | 173.82 | 91.23 | 67381.4 | 329 | 64826.7 | 4.1942 | 21111.2 | 815.56 | 9591.5 | 4116.7 | 111.32 |
| VIC18 | Corinth B | Vilina Cave | Terre. | 2 | 94.8 | 14.17 | 334.63 | 0.72 | 0.81 | 6.78 | 191.94 | 76.21 | 60681.6 | 369.5 | 106063.9 | 3.5668 | 17512.6 | 1113.94 | 9254.9 | 3130.8 | 98.79 |
| VIC19 | Corinth B | Vilina Cave | Terre. | 2 | 105.72 | 16.92 | 313.77 | 0.80 | 0.98 | 8.26 | 153.8 | 95.61 | 69162.6 | 325.4 | 83944.1 | 4.2609 | 21207 | 1028.08 | 8226.5 | 4003.7 | 111.69 |
| VIC2 | Corinth B | Vilina Cave | Terre. | 2 | 103.17 | 16.44 | 228.43 | 0.84 | 0.65 | 8.07 | 130.62 | 83.63 | 69136.3 | 277.7 | 76803.9 | 3.8878 | 19905.3 | 847.65 | 8681.1 | 3802.9 | 106.59 |
| VIC20 | Corinth B | Vilina Cave | Terre. | 2 | 106.43 | 17.84 | 335.59 | 0.87 | 0.93 | 8.84 | 120.12 | 95.08 | 69346.8 | 336.4 | 76296.4 | 4.4188 | 20319.7 | 868.14 | 8952.5 | 4251.3 | 117.18 |
| VIC21 | Corinth B | Vilina Cave | Terre. | Unass. | 110.36 | 15.66 | 221.53 | 0.70 | 0.82 | 7.55 | 173.71 | 69.35 | 63555.1 | 265.6 | 74254.7 | 3.9125 | 19863.5 | 818.29 | 9613.4 | 4021.3 | 125.93 |
| VIC22 | Corinth B | Vilina Cave | Terre. | 2 | 108.94 | 15.85 | 310.55 | 0.72 | 0.62 | 7.70 | 160.77 | 107.07 | 66571.6 | 323.7 | 80081.5 | 3.8461 | 22513.6 | 879.14 | 9207.2 | 3355.6 | 103.42 |
| VIC23 | Corinth B | Vilina Cave | Terre. | 2 | 113.9 | 14.67 | 223.7 | 0.79 | 0.91 | 7.13 | 74.86 | 68.72 | 57181.5 | 326.4 | 61893.5 | 3.1863 | 28098.4 | 630.43 | 9817.6 | 4033.8 | 90.22 |
| VIC24 | Corinth B | Vilina Cave | Terre. | 2 | 63.15 | 15.35 | 259.35 | 0.74 | 0.69 | 7.56 | 679.33 | 83.13 | 68065.8 | 476.9 | 52643.9 | 4.264 | 18426.6 | 506.39 | 7247.9 | 4197.2 | 78.06 |
| VIC25 | Corinth B | Vilina Cave | Terre. | 2 | 110.7 | 15.92 | 307.71 | 0.82 | 0.81 | 7.96 | 101.47 | 81.84 | 60834.8 | 399.6 | 72055.8 | 3.6391 | 22208 | 890.07 | 8746.9 | 3583 | 112.49 |
| VIC26 | Corinth B | Vilina Cave | Terre. | 2 | 92.65 | 16.24 | 286.13 | 0.71 | 1.06 | 7.95 | 143.53 | 85.81 | 65703.2 | 324.4 | 97140.1 | 3.8749 | 17296.4 | 891.68 | 7927 | 3805.1 | 102.36 |
| VIC27 | Corinth B | Vilina Cave | Terre. | 2 | 73.03 | 17.27 | 329.43 | 0.91 | 0.59 | 8.39 | 220.76 | 102.67 | 65418.9 | 325.4 | 83477.4 | 4.2804 | 13338.6 | 841.39 | 7102.1 | 3938.1 | 105.66 |
| VIC28 | Corinth B | Vilina Cave | Terre. | 2 | 90.44 | 16.56 | 200.54 | 0.81 | 0.86 | 7.95 | 256.49 | 77.47 | 68256.8 | 254 | 65558.5 | 3.8583 | 18802.6 | 1306.12 | 9903.6 | 3936.6 | 113.8 |
| VIC29 | Corinth B | Vilina Cave | Terre. | 2 | 101.03 | 15.36 | 305.17 | 0.80 | 0.50 | 7.55 | 157.57 | 114.86 | 60539.1 | 245.6 | 84332.3 | 3.6111 | 21745.9 | 723.81 | 9536 | 3405.4 | 100.13 |
| VIC3 | Corinth B | Vilina Cave | Terre. | 2 | 99.99 | 16.43 | 278.91 | 0.82 | 0.94 | 8.10 | 141.12 | 102.53 | 68002.4 | 292.3 | 77493.3 | 4.2281 | 20717.7 | 706.32 | 9105.5 | 3612.7 | 116.47 |
| VIC30 | Corinth B | Vilina Cave | Terre. | 6 | 78.49 | 16.33 | 308.3 | 0.86 | 0.52 | 8.07 | 158.67 | 64.63 | 65850.6 | 365.5 | 107126.6 | 4.1858 | 16136.3 | 782.74 | 8076.3 | 3909.7 | 124.65 |
| VIC31 | Corinth B | Vilina Cave | Terre. | 6 | 120.39 | 13.26 | 484.48 | 1.03 | 0.84 | 10.03 | 123.3 | 123.86 | 70516.1 | 386.6 | 141503.8 | 4.275 | 14099.2 | 805.79 | 9150.5 | 3266.8 | 82.71 |
| VIC32 | Corinth B | Vilina Cave | Terre. | 2 | 115.68 | 16.80 | 260.63 | 0.87 | 0.63 | 9.04 | 116.61 | 109.91 | 66452.9 | 316.3 | 78614.3 | 3.7074 | 22194 | 951.58 | 11240.2 | 3523.1 | 125.82 |
| VIC4 | Corinth B | Vilina Cave | Terre. | 2 | 88.33 | 17.15 | 247.03 | 0.82 | 0.69 | 8.44 | 174.14 | 106.97 | 62357.4 | 368.8 | 74425.4 | 4.0371 | 21965.4 | 692.08 | 8905.4 | 4115.3 | 111.16 |
| VIC5 | Corinth B | Vilina Cave | Terre. | 2 | 128.41 | 17.70 | 307.01 | 0.89 | 0.93 | 8.30 | 128.29 | 98.13 | 68939.3 | 405.7 | 80806.1 | 4.1626 | 22160.9 | 748.6 | 8536.3 | 4022.4 | 119.89 |
| VIC6 | Corinth B | Vilina Cave | Terre. | 2 | 105.83 | 16.52 | 258.84 | 0.82 | 0.61 | 7.91 | 139.7 | 98.97 | 70118.0 | 384.4 | 75651.4 | 3.5014 | 20952.2 | 740.3 | 9361.5 | 3876.8 | 99.34 |
| VIC7 | Corinth B | Vilina Cave | Terre. | 2 | 113.76 | 16.30 | 283.73 | 0.82 | 0.70 | 7.90 | 107.16 | 85.29 | 68454.2 | 444.3 | 57735 | 3.8733 | 21966.4 | 673.36 | 9342.9 | 3814 | 106.87 |
| VIC8 | Corinth B | Vilina Cave | Terre. | 2 | 82.71 | 17.08 | 348.28 | 0.77 | 0.82 | 7.95 | 81.59 | 85.41 | 77794.8 | 363.5 | 87755.8 | 3.91 | 9935.6 | 706.44 | 12992 | 3617.2 | 126.86 |
| VIC9 | Corinth B | Vilina Cave | Terre. | 2 | 99.72 | 16.38 | 359.33 | 0.72 | 0.92 | 7.70 | 212.66 | 95.83 | 67477.9 | 349.9 | 93726.5 | 3.9836 | 17307.8 | 786.79 | 9554.3 | 3297 | 109.72 |
| VS1 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 38.93 | 11.04 | 471.91 | 0.80 | 0.57 | 7.92 | 82.81 | 99.02 | 55514.4 | 242.8 | 90117.3 | 3.5113 | 10704.1 | 715.07 | 15350.1 | 3141.1 | 97.74 |
| VS10 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 87.59 | 11.41 | 360.42 | 0.96 | 0.61 | 9.28 | 80.82 | 130.49 | 60117.8 | 277.4 | 99880.5 | 4.0061 | 17185.2 | 676.89 | 20315.6 | 3717.4 | 111.06 |
| VS11 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 51.15 | 11.22 | 433.01 | 0.81 | 0.69 | 8.18 | 88.94 | 104.91 | 56458.5 | 276 | 87382.2 | 3.9585 | 12281.6 | 688.41 | 12059.8 | 2627.6 | 83.3 |
| VS12 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 89.4 | 13.78 | 409.79 | 1.14 | 0.76 | 10.76 | 90.49 | 111.55 | 73494.0 | 301.2 | 111662.3 | 4.7363 | 17324 | 722.83 | 14004.3 | 3589.3 | 107.53 |
| VS13 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 66.79 | 11.83 | 251.39 | 0.92 | 0.77 | 8.85 | 98.96 | 101.03 | 63403.5 | 229 | 67479.4 | 4.0445 | 15434.4 | 827.6 | 10157.9 | 2879.1 | 85.52 |
| VS14 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 66.88 | 11.64 | 415.33 | 0.88 | 0.60 | 8.71 | 83.7 | 95.95 | 62648.9 | 234.3 | 95253.7 | 3.7372 | 15692.5 | 595.12 | 8841.1 | 2683.6 | 89.45 |
| VS15 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 50.04 | 11.41 | 390.09 | 0.88 | 0.63 | 8.40 | 84.43 | 103.08 | 60474.8 | 320 | 70318 | 3.6891 | 16315.3 | 729.88 | 10758.4 | 3068.6 | 109.33 |
| VS16 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 87.74 | 10.75 | 455.8 | 0.81 | 0.54 | 7.71 | 81.54 | 127.89 | 56894.1 | 283.9 | 143647 | 3.6033 | 19376.2 | 648.98 | 11692.3 | 2539.7 | 104.7 |
| VS17 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 60.68 | 11.51 | 525.57 | 0.82 | 0.62 | 8.37 | 99.22 | 100.11 | 61537.4 | 290.8 | 120848.8 | 4.0373 | 13669.8 | 713.11 | 8112.8 | 3361.2 | 101.57 |
| VS18 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 78.47 | 11.24 | 367.27 | 0.90 | 0.61 | 8.66 | 83.81 | 95.42 | 63460.5 | 277.8 | 118993.1 | 3.7408 | 15511.5 | 633.63 | 11458.9 | 2941.8 | 82.46 |
| VS19 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 93.56 | 11.13 | 389.06 | 0.92 | 0.67 | 9.11 | 81.97 | 108.24 | 59971.5 | 250.7 | 98109.7 | 4.0336 | 20646 | 671.72 | 18299.8 | 2614.1 | 94.35 |
| VS2 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 61.06 | 11.37 | 437.06 | 0.87 | 0.69 | 8.44 | 94.42 | 71.6 | 58202.8 | 205.9 | 125795.7 | 3.4791 | 13732.6 | 663.49 | 9347.9 | 2763.6 | 89.19 |
| VS20 | Lamboglia | Vela Svitnja | Marine | 1 | 81.21 | 0.00 | 10.75 | 624.30 | 0.79 | 0.57 | 7.42 | 79.67 | 69.9 | 56087.90 | 210.78 | 186250.5781 | 3.48 | 18375.0801 | 718.74 | 8221.87 | 2582.385 |
| VS21 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 50.25 | 11.59 | 626.09 | 0.92 | 0.68 | 8.60 | 91.64 | 100.53 | 59535.0 | 232.6 | 111477.5 | 3.8631 | 7650.9 | 1240.01 | 8471.9 | 3023.7 | 119.87 |
| VS22 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 60.67 | 13.25 | 389.09 | 1.00 | 0.68 | 9.80 | 103.6 | 87.84 | 74263.0 | 347.3 | 78465.6 | 3.9703 | 15648.3 | 704.41 | 9087.3 | 2997.4 | 106.43 |
| VS23 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 103.85 | 14.16 | 485.61 | 1.01 | 0.69 | 10.87 | 103.4 | 121.31 | 78480.0 | 894.8 | 88706.4 | 4.6765 | 19304.9 | 805.56 | 12175.9 | 4032.9 | 124.08 |
| VS24 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 51.5 | 10.50 | 529.91 | 0.92 | 0.64 | 9.76 | 72.22 | 97.36 | 59668.7 | 250.9 | 150250.3 | 4.1004 | 11778.3 | 758.73 | 10975.7 | 3070.5 | 64.94 |
| VS25 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 43.1 | 11.06 | 603.4 | 0.86 | 0.74 | 7.91 | 87.22 | 88.12 | 56302.9 | 229.6 | 119317.8 | 3.7501 | 9969.1 | 701.2 | 9688.8 | 2809.3 | 97.14 |
| VS26 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 80.34 | 11.22 | 458.44 | 0.82 | 0.74 | 8.45 | 80.21 | 103.49 | 55404.5 | 240.8 | 142800.8 | 3.5586 | 18040.4 | 650.77 | 10647.8 | 2823.8 | 89.7 |
| VS27 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 67.08 | 10.25 | 474.28 | 0.81 | 0.76 | 7.68 | 80.03 | 92.73 | 51490.8 | 187.7 | 135472.8 | 3.489 | 15212.2 | 625.29 | 9994.8 | 3032.7 | 111.51 |
| VS28 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 55.37 | 10.05 | 424.18 | 0.72 | 0.58 | 7.71 | 74.63 | 124.03 | 53345.9 | 286.2 | 119984.4 | 3.4848 | 12721.9 | 757 | 11430.8 | 2710.2 | 83.27 |
| VS29 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 76.87 | 12.64 | 463.05 | 0.91 | 0.81 | 8.73 | 94.22 | 122.93 | 63552.8 | 308.6 | 87157.9 | 4.0595 | 14541.8 | 672.62 | 11321.2 | 3722.9 | 108.81 |
| VS3 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 87.19 | 10.81 | 452.47 | 0.88 | 0.56 | 8.33 | 76.23 | 117.54 | 55397.3 | 272.7 | 115741.4 | 3.3491 | 18511 | 827.15 | 13235.1 | 2697.2 | 106.33 |
| VS30 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 106.91 | 12.37 | 468.62 | 1.00 | 0.94 | 9.19 | 83.42 | 129.33 | 60946.5 | 296.2 | 120593.8 | 4.4546 | 22119.5 | 900.56 | 16319.8 | 3047.7 | 108.3 |
| VS31 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 31.34 | 9.90 | 1165.75 | 0.76 | 0.48 | 7.04 | 75.98 | 87.4 | 51969.1 | 285.1 | 193843.3 | 3.5081 | 7016.2 | 671.52 | 13826.8 | 2149.3 | 87.97 |
| VS32 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 50.02 | 9.91 | 1009.02 | 0.74 | 0.51 | 7.24 | 75.7 | 91.3 | 54773.9 | 219.4 | 135194.3 | 3.6616 | 14278.2 | 675.42 | 12228.5 | 2905.2 | 90.18 |
| VS4 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 67.32 | 10.64 | 381.95 | 0.81 | 0.61 | 8.07 | 85.27 | 90.47 | 56256.9 | 217.9 | 120762.3 | 3.6771 | 15466 | 694.06 | 8893.3 | 2912.5 | 94.59 |
| VS5 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 40.65 | 10.88 | 476.45 | 0.81 | 0.53 | 7.90 | 90.44 | 108.99 | 55722.0 | 275.5 | 69697.6 | 3.5753 | 10276.6 | 802.49 | 11298.6 | 2941.7 | 92.48 |
| VS6 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 75.33 | 10.21 | 1151.86 | 0.76 | 0.54 | 7.50 | 79.14 | 114.35 | 53414.0 | 291.9 | 151558.8 | 3.3779 | 16069.5 | 555.46 | 7897.3 | 2831.4 | 95.83 |
| VS7 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 45.8 | 11.23 | 493.41 | 0.84 | 0.61 | 8.14 | 84.04 | 81.08 | 53429.5 | 228.4 | 98340.3 | 3.5104 | 8055.6 | 816.95 | 11925.8 | 2433.5 | 94.63 |
| VS8 | Lamboglia 2 | Vela Svitnja | Marine | Unass. | 79.78 | 14.07 | 539.87 | 1.04 | 0.68 | 10.13 | 96.14 | 96.42 | 72182.3 | 301.4 | 136000.2 | 4.3323 | 17860.2 | 758.59 | 13045.2 | 3606.4 | 108.42 |
| VS9 | Lamboglia 2 | Vela Svitnja | Marine | 1 | 82.57 | 10.69 | 473.45 | 0.80 | 0.63 | 7.82 | 84.37 | 99.09 | 54074.6 | 274.6 | 117410.1 | 3.4569 | 20170.2 | 742.6 | 12254.3 | 2604.8 | 83.6 |
| ZEM1 | Corinth B | Zemunik | Terre. | 4 | 126.38 | 19.39 | 305.72 | 1.12 | 1.07 | 13.42 | 141.2 | 129.04 | 100471.3 | 466.7 | 54243.2 | 5.3995 | 22679.1 | 1025.1 | 11050.5 | 4851.6 | 151.2 |
| ZEM2 | Corinth B | Zemunik | Terre. | 2 | 180.71 | 15.59 | 379.66 | 0.77 | 0.55 | 7.64 | 93.27 | 74.05 | 67243.7 | 430.9 | 95776.8 | 4.1004 | 17417.9 | 817.38 | 12138.7 | 4226 | 109.76 |
| ZEM3 | Corinth B | Zemunik | Terre. | 4 | 138.17 | 20.04 | 250.16 | 1.12 | 1.09 | 14.39 | 148.7 | 126.07 | 103672.1 | 548.5 | 52397.8 | 5.9732 | 23813 | 1226.7 | 13034.2 | 5162.7 | 153.71 |
| ZIR1 | Corinth B | Zirje | Marine | 2 | 41.69 | 12.94 | 424.77 | 0.68 | 0.57 | 6.38 | 93.26 | 74.77 | 51224.5 | 185.9 | 128654.7 | 3.3572 | 10873.8 | 703.33 | 8705.2 | 2644.4 | 91.94 |
| ZIR10 | Corinth B | Zirje | Marine | Unass. | 37.44 | 18.30 | 288.87 | 0.94 | 1.17 | 10.34 | 176.48 | 117.04 | 70209.9 | 263.9 | 84002.4 | 5.4941 | 11828 | 532.87 | 13988 | 3955.7 | 142.64 |
| ZIR11 | Corinth B | Zirje | Marine | 3 | 57.57 | 15.07 | 228.78 | 1.43 | 1.14 | 15.25 | 113.64 | 209.75 | 72278.9 | 189.7 | 49925.6 | 5.1658 | 10184.3 | 1096.61 | 9477.1 | 4236.2 | 119.11 |
| ZIR12 | Corinth B | Zirje | Marine | 3 | 93.73 | 16.44 | 131.33 | 1.10 | 1.11 | 13.18 | 111.63 | 242.28 | 76207.0 | 322.5 | 33195.1 | 5.1376 | 18904.8 | 620.92 | 11292 | 4339.2 | 149.56 |
| ZIR13 | Corinth B | Zirje | Marine | 3 | 84.75 | 16.33 | 185.15 | 1.44 | 1.00 | 15.61 | 128.18 | 253.37 | 85040.9 | 322 | 47578.8 | 5.8878 | 14601.6 | 857.29 | 7174 | 4595.9 | 184.54 |
| ZIR14 | Corinth B | Zirje | Marine | Unass. | 61.16 | 14.93 | 693.29 | 1.13 | 1.07 | 12.36 | 101.75 | 195.54 | 67124.4 | 251.5 | 83381 | 4.7627 | 10937.6 | 864.93 | 9018.2 | 3930.4 | 121.46 |
| ZIR15 | Corinth B | Zirje | Marine | 3 | 55.43 | 15.05 | 259.19 | 1.13 | 0.99 | 12.19 | 102.56 | 180.5 | 74934.2 | 233.9 | 75020.6 | 4.7493 | 12639.1 | 782.29 | 9105.6 | 4135.2 | 107.57 |
| ZIR16 | Corinth B | Zirje | Marine | 2 | 34.62 | 16.44 | 502.32 | 0.77 | 0.61 | 7.98 | 108.75 | 79.59 | 65284.5 | 190.9 | 94280 | 3.729 | 9842.2 | 791.03 | 7211.6 | 3271.2 | 141.53 |
| ZIR17 | Corinth B | Zirje | Marine | 3 | 70.19 | 14.67 | 125.73 | 1.29 | 1.03 | 14.65 | 104.64 | 304.68 | 77009.1 | 269.3 | 29717.3 | 5.2107 | 12935.6 | 864.13 | 9435.3 | 4738.9 | 109.6 |
| ZIR18 | Corinth B | Zirje | Marine | 3 | 59.7 | 17.13 | 110.46 | 1.22 | 1.08 | 13.73 | 119.79 | 171.37 | 79080.5 | 230.3 | 44644.7 | 5.3826 | 16108.4 | 869.16 | 10835.3 | 4706 | 129.62 |
| ZIR19 | Corinth B | Zirje | Marine | Unass. | 52.21 | 11.49 | 468.12 | 0.55 | 0.64 | 5.77 | 83.99 | 82.09 | 46953.3 | 180 | 129638.9 | 2.8582 | 11230.1 | 735.23 | 9970.4 | 2546.1 | 83.84 |
| ZIR2 | Corinth B | Zirje | Marine | 3 | 91.61 | 15.71 | 196.29 | 1.31 | 0.98 | 14.60 | 100.06 | 213.01 | 77708.5 | 282.9 | 56874.7 | 5.5793 | 13036.7 | 1022.7 | 8127.4 | 4240.6 | 112.74 |
| ZIR20 | Corinth B | Zirje | Marine | Unass. | 21.68 | 10.42 | 915.99 | 0.60 | 0.43 | 5.26 | 76.49 | 93.75 | 44865.2 | 137.1 | 140722.9 | 2.7714 | 7663.1 | 398.63 | 9702 | 2440.9 | 98.72 |
| ZIR21 | Corinth B | Zirje | Marine | Unass. | 42.44 | 13.37 | 146.74 | 1.28 | 1.19 | 12.89 | 98.89 | 240.55 | 72064.8 | 153.8 | 31230.3 | 4.8701 | 9236.8 | 956.84 | 10426.7 | 4461.6 | 87.09 |
| ZIR22 | Corinth B | Zirje | Marine | 3 | 96.63 | 16.70 | 194.02 | 1.43 | 1.38 | 15.80 | 117.54 | 180.04 | 93000.3 | 336.3 | 52303.1 | 6.0051 | 14438.3 | 1063.43 | 7540.7 | 5028.1 | 148.77 |
| ZIR3 | Corinth B | Zirje | Marine | 3 | 63.98 | 16.20 | 126.7 | 1.24 | 1.16 | 14.93 | 121.13 | 241.56 | 77469.5 | 208.3 | 39148.5 | 5.6221 | 12018.3 | 1063.71 | 9509.5 | 5051.3 | 125.3 |
| ZIR4 | Corinth B | Zirje | Marine | 2 | 47.2 | 14.96 | 214.02 | 1.22 | 1.16 | 13.99 | 100.56 | 172.46 | 76251.1 | 192.4 | 52137.6 | 5.3376 | 9618.5 | 1033.34 | 9321.6 | 4554.2 | 89.32 |
| ZIR5 | Corinth B | Zirje | Marine | 3 | 30.75 | 13.80 | 44.13 | 1.36 | 1.27 | 15.59 | 107.41 | 247.64 | 74700.0 | 119.3 | 15662.7 | 5.478 | 7223.1 | 637.01 | 9318 | 4749.4 | 82.63 |
| ZIR6 | Corinth B | Zirje | Marine | 3 | 71.91 | 13.28 | 256.84 | 1.12 | 0.90 | 13.13 | 90.5 | 232.76 | 69368.0 | 212.8 | 53363.8 | 4.9326 | 12378.9 | 955.27 | 8172.9 | 4651.8 | 101.56 |
| ZIR7 | Corinth B | Zirje | Marine | 3 | 34.03 | 11.79 | 721.5 | 0.63 | 0.50 | 5.78 | 83.82 | 79.46 | 53053.4 | 163.9 | 127818.1 | 3.0294 | 10478.5 | 640.04 | 8351.8 | 3136.2 | 81.94 |
| ZIR8 | Corinth B | Zirje | Marine | 2 | 29.21 | 11.83 | 563.28 | 0.62 | 0.49 | 5.83 | 87.65 | 69.9 | 47089.9 | 149.9 | 117998.8 | 3.1098 | 8190.1 | 579.72 | 9455.1 | 2799.1 | 88.13 |
| ZIR9 | Corinth B | Zirje | Marine | 3 | 63.27 | 15.99 | 179.37 | 1.33 | 1.20 | 15.38 | 115.29 | 225.06 | 78685.0 | 246.2 | 35875 | 5.6157 | 11150.9 | 979.28 | 8629.7 | 5309.8 | 123.86 |