Supplemental Material for

Push-pull behavior of 2,7-disubstituted sila- and germafluorenes

Shelby J. Jarrett-Noland, William McConnell, Stephan M. Germann, Janet Braddock-Wilking, and Cynthia M. Dupureur*

Fig. S1 Absorbance spectra of Compounds a-d in the presence of the indicated solvents. Compounds b, c, and d are at 2 mM; compound a is at 4 mM. Compound a is not sufficiently soluble in MeOH on this scale.

Table S1. Polarizability Functions for Bakhshiev and Kawski-Chamma-Viallet plotsa

| Solvent | f2(ϵ,η) | f3(ϵ,η) |
| --- | --- | --- |
| Toluene Chloroform DCM Acetone Methanol DMSO | 0.0297 0.3714 0.5904 0.7903 0.8555 0.8405 | 0.3542 0.5474 0.6804 0.7783 0.8065 0.8759 |

aFrom Eqns. 5 and 6. Solvent dielectric constants and refractive indices are from Ref. [1]

and [2].

Fig. S2 Bakhshiev plots for Compounds a-d. Stokes shift derived from absorption and emission maxima (Fig. 4 and 5) of compounds a-d in wavenumbers (cm-1). Orientation polarizability calculated from Eq 6.  Conditions: 1 mM MF at 25 °C.

Fig. S3 Kawski-Chamma-Viallet plots for Compound a-d. Stokes shift derived from absorption and emission maxima (Fig. 4 and 5) of compounds a-d in wavenumbers (cm-1). Orientation polarizability calculated from Eq 7.  Conditions: 1 mM MF at 25 ˚C.  Note that the y axis is different than for Lippart-Mataga and Bakhshiev plots. Here error bars are too small to be visible.

Table S2  Dipole Moments of Sila- and Germafluorenes in Debye

| Compound | Onsager Radius, Åa | ∆μLM b | ∆μBKc | ∆μKCVd | μgDFTe | μgf | μeDFTg | μeh |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| a | 8.331 | 4.10 | 2.55 | 3.42 | 2.96 | 2.60 | 0.94 | 0.832 |
| b | 8.285 | 2.98 | 1.73 | 2.21 | 3.24 | 0.137 | 3.93 | 2.332 |
| c | 6.608 | 1.89 | 1.21 | 1.64 | 1.98 | 2.26 | 1.93 | 0.613 |
| d | 6.166 | 2.43 | 1.37 | 1.67 | 2.23 | 2.59 | 2.90 | 1.216 |

aOnsager radius; bChange in magnitude of the dipole moment from Eq. 2; cChange in magnitude of the dipole moment from Eq. 9; dChange in dipole moment from Eq. 10; eGround state dipole moment derived from DFT in polar solvent; reproduced from Table 3; fGround state dipole moment from Eq. 11; reproduced from Table 3; gExcited state dipole moment from DFT calculations in DMF; hExcited state dipole moment from Eq. 12

REFERENCES

[1] Handbook of Chemistry and Physics, 87th ed., CRC Press, 2006.

[2] M. Polyanskiy, Refractive index database, https://refractiveindex.info. Accessed on 2022-05-20., (2022).