Supplementary Materials

Strong and tough Mg-MAX phase composites with nacre-like lamellar and brick-and-mortar architectures

Yanyan Liu1,2,#, Xi Xie2,#, Zengqian Liu1,2,*, Qin Yu3, Xuegang Wang2, Qing Jia1,2, Zhefeng Zhang1,2,*, Rui Yang2,4,*, Robert O. Ritchie3

1School of Materials Science and Engineering, University of Science and Technology of China, Shenyang 110016, China

2Shi-Changxu Innovation Center for Advanced Materials, Institute of Metal Research, Chinese Academy of Sciences, Shenyang 110016, China

3Department of Materials Science and Engineering, University of California Berkeley, Berkeley, CA 94720, USA

4Center for Adaptive System Engineering, School of Creativity and Art, ShanghaiTech University, Shanghai 201210, China

____________

#These authors contributed equally to this work.

*Corresponding authors: Tel: +86-24-8397-0116, e-mail address: zengqianliu@imr.ac.cn (Z. Liu); Tel: +86-24-2397-1043, e-mail address: zhfzhang@imr.ac.cn (Z. Zhang); Tel: +86-21-2068-4099, e-mail address: yangrui@shanghaitech.edu.cn (R. Yang).

Figure S1. Distribution of elements measured by EDS in the pure Mg composite with lamellar architecture. The Mg element and the elemental Ti, Al and C were found to be principally concentrated in the metal and ceramic-rich constituents, respectively, which is similar with the case in the AZ91D composites.

Figure S2. Crack bifurcation and deflection in the nacre-like Mg-MAX phase composites. Plastic deformation and microcracking occurred around the crack tip and played a role in promoting the crack bifurcation and deflection following the slip bands in the inter-lamellar regions or along the microcracks. The AZ91D alloy composite with lamellar architecture was taken as an example here.

Figure S3. Representative room temperature tensile stress-strain curves of pure Mg and AZ91D alloy which were solidified following the same process as for the melt infiltration procedure of the Mg-MAX phase composites.