Copper Adorned Magnetic Nanoparticles as a Heterogeneous Catalyst for Sonogashira Coupling Reaction in Aqueous Media

Safoora Sheikh 1,2*, Mohammad Ali Nasseri 1*, Ali Allahresani 1,  and Rajender S. Varma3

1Department of Chemistry, Faculty of Basic Sciences, University of Birjand, P. O. Box 97175-615, Birjand, Iran

2Institut für Organische Chemie, Universität Regensburg, Universitätsstr. 31, 93053 Regensburg, Germany

3Regional Centre of Advanced Technologies and Materials, Czech Advanced Technology and Research Institute, Palacký University in Olomouc, ˇSlechtitelů 27, 783 71, Olomouc, Czech Republic.

*To whom correspondence should be addressed:

*sheikhsafoora90@gmail.com; Safoora.sheikh@chemi.uni_regensburg.de (S. Sheik)

*manaseri@birjand.ac.ir; Tel: +98-561-32202065 (M. A. Nasseri)

General

All starting materials were commercially available and were utilized as received. Thin layer chromatography (TLC) was performed on silica–gel 60 F254 plates and UV light was used for visualization. Melting points were determined on a Tropical Labequip apparatus. The FT–IR spectra (JASCO–FT–IR 4600) were recorded using KBr pellet. The 1H–NMR and 13C–NMR spectra were recorded on a Bruker Avance DPX–300 spectrometer in the deuterated solvents (CDCl3), using tetramethylsilane (TMS) as an internal standard. The Field emission scanning electron microscopy (FE–SEM) images of the prepared catalysts were recorded on a Tescan MIRA3. EDX analysis were performed using a FESEM (JEOL–7600F–Oxford) equipped with a spectrometer of energy dispersion of X–ray. The presence of the elements was confirmed using the point elemental mapping (Tescan–Mira 3–SAMX). Liquid chromatography–mass spectrometry for the PAMAM dendrimer G1 was recorded by LC–Mass–AB SCIEX–Q–trap 3200 instrument. The microscopic images and size distribution of the catalyst NPs were performed using TEM (Philips–EM208) operating at 100 kV voltage. The X‒ray diffraction (XRD) pattern were recorded by an X’pertpro (Philips) instrument employing Cu Kα radiation (λ = 1.5418 Å), at a scanning speed of 2 °C/min from 10 to 80 °C (2θ). TGA analysis of the samples were performed using a Q600 model from TA company under nitrogen atmosphere with a heating rate of 15 C/min in the temperature range of 25–800 C. The content of Pd in the catalyst was determined by OPTIMA 7300DV ICP analyzer. All the measured yields refer to the isolated products after purification by column chromatography. All the products were  characterized by NMR spectroscopy.

Figure S1. Williamson Hall plot, determination size and strain of γ-Fe2O3@PEG@PAMAM G0-Cu 
MNPs.

Spectra data for the Sonogashira cross-coupling products:

1,2-diphenylacetylene (1a). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with iodobenzene (204.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 94% (175.9 mg) 1,2-diphenylacetylene (1a). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 7.23-7.47 (m, 10H); 13C-NMR (62.9 MHz, CDCl3) δ 89.5, 123.3, 128.3, 129.2, 131.6.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with bromobenzene (157.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 80% (149.7 mg) 1,2-diphenylacetylene (1a). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 7.23-7.45 (m, 10H); 13C-NMR (62.9 MHz, CDCl3) δ 89.5, 123.4, 128.1, 129.6, 131.7.

4-(phenylethynyl)aniline (1b). This compound is well known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 4-iodoaniline (219.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 88% (122.3 mg) 4-(phenylethynyl)aniline (1b). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 3.62 (s, 2H, NH2), 6.52-7.40 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.3, 90.2, 112.5, 114.7, 123.9, 127.7, 128.3, 131.3, 132.9, 146.7.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 4-bromoaniline (172.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 75% (144.7 mg) 4-(phenylethynyl)aniline (1b). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 3.62 (s, 2H, NH2), 6.53-7.42 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.5, 90.2, 112.3, 114.8, 123.7, 127.7, 128.1, 131.3, 132.9, 146.4.

1-methoxy-4-(phenylethynyl)benzene (1c). This compound is known in the literature [2].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-iodo-4-methoxybenzene (234.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 83% (172.6 mg) 1-methoxy-4-(phenylethynyl)benzene (1c). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 3.76 (s, 3H, CH3), 6.79-7.44 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 55.2, 88.0, 89.4, 114.0, 115.3, 123.6, 127.9, 128.3, 131.4, 133.0, 159.6.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-bromo-4-methoxybenzene (187.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 68% (141.4 mg) 1-methoxy-4-(phenylethynyl)benzene (1c). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 3.72 (s, 3H, CH3), 6.75-7.44 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 55.2, 88.1, 89.3, 114.3, 115.4, 123.5, 127.9, 128.7, 131.5, 133.3, 159.8.

1-methoxy-2-(phenylethynyl)benzene (1d). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 2-iodoanisole (243.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 80% (166.5 mg) 1-methoxy-2-(phenylethynyl)benzene (1d). Chromatography: n-hexane/EtOAc, 8:2. 1H NMR (250 MHz, CDCl3) δ 3.82 (s, 3H, CH3), 6.87-7.53 (m, 9H, Ar-H); 13C NMR (CDCl3, 62.9 MHz) δ 55.8, 85.6, 93.3, 110.6, 112.4, 120.4, 123.5, 128.0, 128.1, 129.7, 131.6, 133.5, 159.8.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 2-bromoanisole (187.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 50% (104.1 mg) 1-methoxy-2-(phenylethynyl)benzene (1d). Chromatography: n-hexane/EtOAc, 8:2. 1H NMR (250 MHz, CDCl3) δ 3.83 (s, 3H, CH3), 6.89-7.56 (m, 9H, Ar-H); 13C NMR (CDCl3, 62.9 MHz) δ 55.9, 85.4, 93.0, 110.4, 112.6, 120.3, 123.2, 128.0, 128.4, 129.7, 131.8, 133.6, 159.7.

1-methyl-4-(phenylethynyl)benzene (1e). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-iodo-4-methylbenzene (218.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 90% (172.8 mg) 1-methyl-4-(phenylethynyl)benzene (1e). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (CDCl3, 250 MHz) δ 2.22 (s, 3H, CH3), 7.14-7.42 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 21.5, 88.7, 89.6, 120.2, 123.5, 128.1, 128.3, 129.1, 131.5, 131.7, 138.4.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-bromo-4-methylbenzene (171.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 78% (149.7 mg) 1-methyl-4-(phenylethynyl)benzene (1e). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (CDCl3, 250 MHz) δ 2.24 (s, 3H, CH3), 7.15-7.41 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 21.8, 88.9, 89.5, 120.1, 123.7, 128.2, 128.3, 129.1, 131.6, 131.8, 138.4.

1-methyl-2-(phenylethynyl)benzene (1f). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-iodi-2-methylbenzene (218.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 80% (153.6 mg) 1-methyl-2-(phenylethynyl)benzene (1m). Chromatography: n-hexane/EtOAc, 8:2. 1H NMR (250 MHz, CDCl3) δ 2.35 (s, 3H, CH3), 7.14-7.45 (m, 9H, Ar-H); 13C NMR (CDCl3, 62.9 MHz) δ 21.5, 88.5, 120.3, 123.6, 128.2, 128.3, 129.4, 131.3, 131.7, 138.7.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-bromo-2-methylbenzene (171.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 50% (96.0 mg) 1-methyl-2-(phenylethynyl)benzene (1f). Chromatography: n-hexane/EtOAc, 8:2. 1H NMR (250 MHz, CDCl3) δ 2.35 (s, 3H, CH3), 7.16-7.45 (m, 9H, Ar-H); 13C NMR (CDCl3, 62.9 MHz) δ 21.5, 88.6, 120.3, 123.6, 128.1, 128.3, 129.2, 131.4, 131.7, 138.5.

1-chloro-4-(phenylethynyl)benzene (1g). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-chloro-4-iodobenzene (238.4 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 80% (170.0 mg) 1-chloro-4-(phenylethynyl)benzene (1g). Chromatography: n-hexane/EtOAc, 8:2. 1H NMR (250 MHz, CDCl3) δ 7.13-7.43 (m, 9H, Ar-H) ppm; 13C NMR (62.9 MHz, CDCl3) δ 88.2, 90.3, 121.8, 122.9, 128.4, 128.5, 128.7, 131.6, 132.8, 134.2.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-brom-4-iod-benzol (282.9 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 60% (127.5 mg) 1-chloro-4-(phenylethynyl)benzene (1g). Chromatography: n-hexane/EtOAc, 8:2. 1H NMR (250 MHz, CDCl3) δ 7.14-7.42 (m, 9H, Ar-H); 13C NMR (62.9 MHz, CDCl3) δ 88.1, 90.5, 121.9, 122.9, 128.3, 128.5, 128.8, 131.5, 132.8, 134.3.

4-(phenylethynyl)benzaldehyde (1h). This compound is known in the literature [3].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 4-iodobenzaldehyde (232.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 92% (189.7 mg) 4-(phenylethynyl)benzaldehyde (1h). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (CDCl3, 250 MHz) δ 7.36-7.87 (m, 9H, Ar-H), 10.01 (s, 1H); 13C-NMR (62.9 MHz, CDCl3) δ 88.4, 93.3, 122.4, 128.4, 128.8, 129.5, 131.7, 132.0, 153.2.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 4-bromobenzaldehyde (185.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 80% (164.9 mg) 4-(phenylethynyl)benzaldehyde (1h). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (CDCl3, 250 MHz) δ 7.36-7.87 (m, 9H, Ar-H), 10.03 (s, 1H); 13C-NMR (62.9 MHz, CDCl3) δ 88.4, 93.1, 122.3, 128.2, 128.4, 129.5, 131.5, 132.6, 153.1.

methyl 4-(phenylethynyl)benzoate (1i). This compound is known in the literature [3].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with methyl-4-iodobenzoat (262.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 90% (212.5 mg) methyl 4-(phenylethynyl)benzoate (1i). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (CDCl3, 250 MHz) δ 3.39 (s, 3H), 7.36-8.08 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 53.2, 88.8, 92.5, 122.8, 128.2, 128.9, 129.7, 131.5, 131.9, 166.5.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with methyl-4-bromobenzoate (215.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 73% (172.4 mg) methyl 4-(phenylethynyl)benzoate (1i). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (CDCl3, 250 MHz) δ 3.39 (s, 3H), 7.35-8.07 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 53.1, 88.6, 92.4, 122.8, 128.4, 128.9, 129.6, 131.5, 131.8, 166.5.

1-(4-(phenylethynyl)phenyl)ethanone (1j). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-(4-iodophenyl)ethanone (246.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 93% (204.7 mg) 1-(4-(phenylethynyl)phenyl)ethanone (1j). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 2.51 (s, 3H, CH3), 7.16- 7.86 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 27.0, 88.9, 92.9, 123.0, 128.2, 128.3, 128.8, 129.5, 132.0, 132.2, 136.5, 197.6.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-(4-bromophenyl)ethanone (199.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 75% (165.1 mg) 1-(4-(phenylethynyl)phenyl)ethanone (1j). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 2.52 (s, 3H, CH3), 7.14- 7.85 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 27.2, 88.8, 92.9, 123.3, 128.1, 128.2, 128.7, 129.6, 132.0, 132.2, 136.4, 197.5.

4-(phenylethynyl)benzonitrile (1k). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 4-iod-benzonitril (229.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 78% (158.4 mg) 4-(phenylethynyl)benzonitrile (1k). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 7.28-7.51 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.8, 93.6, 111.8, 118.4, 122.1, 128.2, 128.5, 129.3, 131.7, 132.0, 132.0.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 4-bromo-benzonitril (182.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 65% (132.0 mg) 4-(phenylethynyl)benzonitrile (1k). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 7.28-7.53 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.7, 93.7, 111.4, 118.5, 122.2, 128.2, 128.5, 129.1, 131.7, 132.03, 132.06.

1-nitro-4-(phenylethynyl)benzene (1l). This compound is known in the literature [1].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-iodo-4-nitrobenzene (249.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 70% (156.2 mg) 1-nitro-4-(phenylethynyl)benzene (1l). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 7.37-8.22 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.5, 94.7, 122.0, 123.6, 128.5, 129.2, 130.2, 131.8, 132.2, 146.9.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-bromo-4-nitrobenzene (202.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 54% (120.5 mg) 1-nitro-4-(phenylethynyl)benzene (1l). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (250 MHz, CDCl3) δ 7.36-8.22 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.4, 94.6, 122.2, 123.8, 128.6, 129.1, 130.1, 131.5, 132.2, 146.8.

1-nitro-3-(phenylethynyl)benzene (1m). This compound is known in the literature [4].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-iodo-3-nitrobenzene (249.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 55% (122.7 mg) 1-nitro-3-(phenylethynyl)benzene (1m). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (400 MHz, CDCl3) δ 7.34-8.28 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.5, 89.8, 120.2, 121.7, 123.0, 124.2, 125.5, 126.2, 127.5, 133.1, 136.5, 149.4.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-bromo-3-nitrobenzene (202.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 45% (100.4 mg) 1-nitro-3-(phenylethynyl)benzene (1m). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (400 MHz, CDCl3) δ 7.36-8.29 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.5, 89.9, 120.-, 121.6, 123.2, 124.2, 125.8, 126.0, 127.4, 133.1, 136.5, 149.5.

1-nitro-2-(phenylethynyl)benzene (1n). This compound is known in the literature [5].

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-iodo-2-nitrobenzene (249.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 65% (145.0 mg) 1-nitro-2-(phenylethynyl)benzene (1n). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (400 MHz, CDCl3) δ 7.35-8.06 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.5, 89.8, 120.2, 121.7, 123.0, 124.2, 125.5, 131.2, 131.8, 132.3, 134.5, 149.3.

Phenylacetylene (153.1 mg, 1.5 mmol) was reacted with 1-bromo-2-nitrobenzene (202.0 mg, 1.00 mmol), NaOH (80.0 mg, 2.00 mmol) and γ-Fe2O3@PEG@THMAM-Co (0.8 mol%, 0.006 g) in water (5 mL) at 80 °C to yield 45% (100.4 mg) 1-nitro-2-(phenylethynyl)benzene (1n). Chromatography: n-hexane/EtOAc, 8:2. 1H-NMR (400 MHz, CDCl3) δ 7.35-8.08 (m, 9H, Ar-H); 13C-NMR (62.9 MHz, CDCl3) δ 87.5, 89.9, 120.0, 121.4, 123.2, 124.2, 125.5, 131.5, 131.9, 132.3, 134.5, 149.1.

References

[1] M. Kazemnejadi, Z. Rezazadeh, M.A. Nasseri, A. Allahresani, M. Esmaeilpour, Imidazolium chloride-Co (iii) complex immobilized on Fe3O4@SiO2 as a highly active bifunctional nanocatalyst for the copper-, phosphine-, and base-free Heck and Sonogashira reactions, Green Chemistry, 21 (2019) 1718-1734.

[2] A.R. Sardarian, M. Kazemnejadi, M. Esmaeilpour, Bis-salophen palladium complex immobilized on Fe3O4@SiO2 nanoparticles as a highly active and durable phosphine-free catalyst for Heck and copper-free Sonogashira coupling reactions, Dalton Transactions, 48 (2019) 3132-3145.

[3] S. Yu, J. Wu, X. He, Y. Shang, Ferrocenyl bisoxazoline as an efficient non‐phosphorus ligand for palladium‐catalyzed copper‐free Sonogashira reaction in aqueous solution, Applied Organometallic Chemistry, 32 (2018) e4156.

[4] A.S. Roy, J. Mondal, B. Banerjee, P. Mondal, A. Bhaumik, S.M. Islam, Pd-grafted porous metal–organic framework material as an efficient and reusable heterogeneous catalyst for C–C coupling reactions in water, Applied Catalysis A: General, 469 (2014) 320-327.

[5] M.A. Nasseri, Z. Rezazadeh, M. Kazemnejadi, A. Allahresani, A Co–Cu bimetallic magnetic nanocatalyst with synergistic and bifunctional performance for the base-free Suzuki, Sonogashira, and C–N cross-coupling reactions in water, Dalton Transactions, 49 (2020) 10645-10660.