| 1c: Hal: I, 88%, 4h, TON: 1110 1c: Hal: Br, 68%, 5.5h, TON: 85 | 1b: Hal: I, 88%, 5h, TON: 110 1b: Hal: Br, 75%, 6h, TON: 93 | 1a: Hal: I, 94%, 3h, TON: 117.5 1a: Hal: Br, 80%, 5h, TON: 100 |  |
| --- | --- | --- | --- |
| 1f: Hal: I, 80%, 4h, TON: 100 1f: Hal: Br, 50%, 5.5h, TON: 62 | 1e: Hal: I, 90%, 3h, TON: 112 1e: Hal: Br, 78%, 6h, TON: 97 | 1d: Hal: I, 80%, 5h, TON: 100 1d: Hal: Br, 50%, 5h, TON: 62 |  |
| 1i: Hal: I, 90%, 6h, TON: 112 1i: Hal: Br, 73%, 4h, TON: 91 | 1h: Hal: I, 92%, 5h, TON: 115 1h: Hal: Br, 80%, 5h, TON: 100 | 1g: Hal: I, 80%, 5h, TON: 100 1g: Hal: Br, 60%, 8h, TON: 75 |  |
| 1l: Hal: I, 70%, 5h, TON: 87 1l: Hal: Br, 54%, 6h, TON: 72 | 1k: Hal: I, 78%, 4.5h, TON: 97 1k: Hal: Br, 65%, 5h, TON: 81 | 1j: Hal: I, 93%, 5h, TON: 116 1j: Hal: Br, 75%, 7h, TON: 93 |  |
|  | 1n: Hal: I, 65%, 4h, TON: 81 1n: Hal: Br, 45%, 4h, TON: 56 | 1m: Hal: I, 55%, 6h, TON: 68 1m: Hal: Br, 45%, 5h, TON: 56 |  |
| Table 2. Sonogashira coupling reactions of different aryl halides with phenylacetylene catalyzed by γ-Fe2O3@PEG@PAMAM G0-Cu.a aReaction conditions: aryl halide (1.00 mmol), phenylacetylene (1.5 mmol), NaOH (2.00) mmol, catalyst (0.006 g, 0.8 mol% Co), H2O (5.0 mL), 80 oC; All yields are Isolated. |  |  |  |

| Ref. | Yieldb (%) | Time (h) | Reaction conditions | Catalyst (mol%) | Entry |  |
| --- | --- | --- | --- | --- | --- | --- |
| 36 | 43 | 24 | K2CO3/PPh3 (4 mol%)/H2O/140 °C | CuI (0.2 mol%) | 1 |  |
| 37 | 71 | 8 | K2CO3/DMF/125 °C | NHC precursor (20 mol%)/CuSO4·5H2O (20 mol%)c | 2 |  |
| 38 | 82 | 8 | K2CO3/DMF/ethylene glycol/r.t | Co(C9H9NO2)3 | 3 |  |
| 39 | 72 | 10 | KOH/DMSO/140 °C | MNPs@Cs-MS-Co (0.55 mol%)d | 4 |  |
| 40 | 54 | 15 | K2CO3/EtOH/r.t | CuO/TiO2 | 5 |  |
| 41 | 99 | 8 | Cs2CO3/DMF/60 °C | Pd3Cu1/SiC | 6 |  |
| 42 | 90 | 36 | K2CO3/DMF/120 °C | Cu(OAc)2 (10 mol%)/β-diketone | 7 |  |
| 43 | 76 | 24 | NaOH/H2O/100 °C | Cu-Salen (10 mol%)/PTCe | 8 |  |
| 44 | 94 | 2 | KOH/DMF/140 °C | Cu (10 mol%)/DABCO@SiOf | 9 |  |
| This work | 94 | 3 | NaOH/H2O/80 °C | γ-Fe2O3@PEG@PAMAM G0-Cu | 10 |  |
| Table 4 Catalytic activity of the γ-Fe2O3@PEG@PAMAM-Co MNPs was compared with reported catalysts for the Sonogashira cross coupling reaction (1a). a Sonogashira: reaction of iodobenzene and phenyl acetylene, b Isolated yield, c NHC: N-heterocyclic carbine, d MNPs@Cs-MS-Co: cobalt tagged on MNPs-chitosan functionalized with methyl salicylate, e PTC: phase-transfer catalyst. |  |  |  |  |  |  |