Effective Remediation of Pb2+ Polluted Environment by Adsorption onto Recyclable Hydroxyl Bearing Covalent Organic Framework

Ahmed M. Elewa,a,b Ahmed F. M. EL-Mahdy,c,* and Ho-Hsiu Chou a,*

aDepartment of Chemical Engineering, National Tsing Hua University, Hsinchu 300044, Taiwan

bNuclear Chemistry Department, Hot Laboratories Center, Atomic Energy Authority, P.O. Box 13759, Inshas, Cairo, Egypt

cDepartment of Materials and Optoelectronic Science, National Sun Yat-Sen University, Kaohsiung, 80424, Taiwan

E-mail: hhchou@mx.nthu.edu.tw

S1. Materials

Lead (II) nitrate (Pb(NO3)2) and p-Formylbenzeneboronic acid were purchased from Sigma-Aldrich. 2,5-Dihydroxyterephthalic acid, Tetrakis(triphenylphosphine) palladium(0), and 1,3,5-tribromobenzene were purchased from Acros. Hydrazine hydrate (98%), mesitylene, and potassium carbonate were obtained from Alfa Aesar. Analytical grade methanol, ethanol, 1,4-dioxane, glacial acetic acid, and acetone were obtained and utilized without purification.

S2. Characterization

Siemens D5000 and monochromated Cu/K (= 0.1542 nm) were used for determining the COFs' powder X-ray diffraction (PXRD) pattern. On an XRD sample holder's square recess, the sample was dispersed thinly. The FTIR spectra were acquired using the KBr plate approach on a Bruker Tensor 27 FTIR spectrophotometer; 32 scans were made at a resolution of 4 cm–1. The surface area and porosity of the prepared samples (ca. 20–100 mg) were measured using a Micromeritics ASAP 2020 Surface Area and Porosity analyzer. Nitrogen gas isotherm was created by gradually exposing a liquid N2 (77 K) bath to ultrahigh-purity N2 (up to 1 atm). Under a flowing N2 environment, TGA was conducted with a TA Q-50 analyzer. The material was packed in a Pt cell and heated at a rate of 20 °C min–1 under N2 at a flow rate of 50 mL min–1 from 40 to 800 °C. A JEOL-2100 scanning electron microscope with a 200 kV accelerating voltage was used for transmission electron microscopy (TEM). A JEOL JSM-7610F scanning electron microscope was used to perform field-emission scanning electron microscopy (FE-SEM); the COF sample was sputtered with Pt for 100 seconds prior to imaging. A SUNTEX SP-2100 pH meter was used to take all of the readings.

S3. Synthetic Procedures

S3.1. Synthesis of 2,3-dihydroxybenzene-1,4-dicarbohydrazide (DHTP). Hydrazine monohydrate (5mL) and diethyl 2,5-dihydroxyterephthalate (1.00 g, 3.93 mmol) and 40 mL ethanol were charged into a 200 mL round-bottom flask, then heated the mixture under reflux for 24 h at 90 °C. The pale-yellow precipitate was filtered and washed several times with ethanol. After recrystallizations of the crude solid from ethanol, DHTP (0.75 g, 86%) was produced.

Scheme S1 Synthesis of 2,5-dihydroxyterephthalohydrazide (DHTP)

S3.2. Synthesis of 1,3,5-tris (4'-aldehyde phenyl) benzene (TPB–3CHO). 1,3,5-tribromobenzene (0.75 g, 2.38 mmol), 4-(Dihydroxyboryl)benzaldehyde (2.145 g, 14.32 mmol), tetrakis(triphenylphosphine) palladium(0) (138 mg, 0.12 mmol), and potassium carbonate (1.98 g, 14.32 mmol) were charged into a 100 mL round-bottom flask, then evacuated under pressure for 15 min and then a mixture of 30 mL of 1,4-dioxane and 5.5 mL of water was added slowly under N2. The resultant mixture was heated for 40 h at 110 °C before cooling to room temperature. A white precipitate formed when the mixture was put into 200 mL of ice water. The crude material was washed with water and MeOH multiple times after vacuum filtering. TPB–3CHO was obtained as a white solid after purification using a flash chromatographic column (SiO2; EA/n-hexane, 1: 9) (743 mg, 80%).

Scheme S2 Synthesis of 1,3,5-tris(4-formylphenyl)benzene (TPB-3CHO)

S3.3. Preparation of DHTP–TPB COF. TPB–3CHO (75 mg, 0.192 mmol) and DHTP (65.2 mg, 0.288 mmol) are charged into a Pyrex tube together with mesitylene and 1,4-dioxane (3: 1, 4 mL) and an aqueous solution of acetic acid (6 M, 0.4 mL). To achieve a uniform dispersion, this mixture was sonicated for 15 minutes. After many freeze/pump/thaw cycles, the tube was capped and degassed before being heated at 120 °C for 72 hours. After cooling to ambient temperature, the yellow-brownish solid was filtered and washed with THF, MeOH, and acetone. After drying under vacuum at 120 °C for 24 hours, the DHTP–TPB COF solid (90 % yield) was produced.

S4. Spectral Profiles of monomers

Fig. S1 FT-IR spectrum of 2,5-dihydroxyterephthalohydrazide (DHTP)

Fig. S2 1H NMR spectrum of 2,5-dihydroxyterephthalohydrazide (DHTP)

Fig. S3 13C NMR spectrum of 2,5-dihydroxyterephthalohydrazide (DHTP)

Fig. S4 FT-IR spectrum of 1,3,5-tris(4-formylphenyl)benzene (TPB-3CHO)

Fig. S5 1H NMR spectrum of 1,3,5-tris(4-formylphenyl)benzene (TPB-3CHO)

Fig. S6 13C NMR spectrum of 1,3,5-tris(4-formylphenyl)benzene (TPB-3CHO)

Fig. S7 (a) Pictorial representation for batch adsorption of Pb2+ onto DHTP–TPB COF, (b) the best condition for Pb2+ adsorption onto DHTP–TPB COF.

S5. PXRD data and BET parameters

Table S1. PXRD and BET parameters of the synthesized COF

| COF | SBET (m2 g-1) | d100 (nm) | Pore size (nm) | Pore volume (cm3 g-1) | Interlayer Distance (Å) |
| --- | --- | --- | --- | --- | --- |
| DHTP–TPB | 360 | 4.01 | 3.77 | 0.58 | 3.45 |

S6. Structural Modeling and Fractional Atomic Coordinates for COF Structure

Fig. S8 Crystalline structure for the DHTP–TPB COF (a, b) completely eclipsed AA-stacking models and (c, d) staggered AB-stacking successions models

Table S2. Fractional atomic coordinates for the unit cell of the DHTP–TPB COF with eclipsed AA-stacking model

| Sample Name: DHTP–TPB COF |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Space Group: P 1 |  |  |  |  |  |  |  |
| a = 46.23100 , b = 46.23100, c = 4.07851 α = β = 90°, γ = 120° |  |  |  |  |  |  |  |
| Rwp= 4.91% Rp= 3.72% |  |  |  |  |  |  |  |
| Atom | x/a | y/b | z/c | Atom | x/a | y/b | z/c |
| C1 | 0.60426 | 0.16673 | 0.5738 | C30 | 0.46226 | 0.45959 | 0.25054 |
| C2 | 0.63673 | 0.19111 | 0.65973 | C31 | 0.48424 | 0.44661 | 0.26022 |
| C3 | 0.65015 | 0.22492 | 0.58724 | C32 | 0.51808 | 0.46671 | 0.34016 |
| C4 | 0.63177 | 0.23618 | 0.42363 | C33 | 0.52917 | 0.50025 | 0.42553 |
| C5 | 0.59947 | 0.21165 | 0.32712 | C34 | 0.50722 | 0.51309 | 0.4148 |
| C6 | 0.58584 | 0.17733 | 0.40141 | C35 | 0.3656 | 0.59073 | 0.29195 |
| C7 | 0.64626 | 0.27342 | 0.37002 | C36 | 0.3855 | 0.57542 | 0.31643 |
| C8 | 0.68111 | 0.29453 | 0.33079 | C37 | 0.41322 | 0.58845 | 0.50815 |
| C9 | 0.69591 | 0.32958 | 0.30566 | C38 | 0.42057 | 0.61732 | 0.67092 |
| C10 | 0.67483 | 0.34363 | 0.31535 | C39 | 0.40109 | 0.63278 | 0.6441 |
| C11 | 0.63981 | 0.32357 | 0.35304 | C40 | 0.37315 | 0.6198 | 0.45534 |
| C12 | 0.62599 | 0.2884 | 0.37741 | C41 | 0.39172 | 0.74692 | 0.30685 |
| C13 | 0.73343 | 0.35151 | 0.27487 | C42 | 0.40689 | 0.782 | 0.34308 |
| C14 | 0.75573 | 0.34509 | 0.4376 | C43 | 0.39395 | 0.79577 | 0.54594 |
| C15 | 0.7907 | 0.36565 | 0.4086 | C44 | 0.36507 | 0.77355 | 0.70481 |
| C16 | 0.80453 | 0.39298 | 0.21231 | C45 | 0.34959 | 0.73876 | 0.66409 |
| C17 | 0.78231 | 0.39921 | 0.04827 | C46 | 0.36282 | 0.72468 | 0.46771 |
| C18 | 0.74743 | 0.37907 | 0.08071 | C47 | 0.31649 | 0.61655 | 0.4326 |
| C19 | 0.61798 | 0.33947 | 0.38123 | C48 | 0.35178 | 0.63618 | 0.43683 |
| C20 | 0.62477 | 0.36861 | 0.22251 | C49 | 0.36648 | 0.67142 | 0.43972 |
| C21 | 0.60444 | 0.38338 | 0.2541 | C50 | 0.34683 | 0.68705 | 0.44126 |
| C22 | 0.57668 | 0.36946 | 0.44562 | C51 | 0.31162 | 0.66652 | 0.43353 |
| C23 | 0.57005 | 0.34051 | 0.60386 | C52 | 0.29576 | 0.63115 | 0.43066 |
| C24 | 0.59028 | 0.3259 | 0.57316 | C53 | 0.2065 | 0.55569 | 0.34482 |
| C25 | 0.43456 | 0.5726 | 0.55288 | C54 | 0.24137 | 0.5767 | 0.31905 |
| C26 | 0.55389 | 0.38371 | 0.48768 | C55 | 0.25777 | 0.60946 | 0.43623 |
| C27 | 0.54222 | 0.45405 | 0.30016 | C56 | 0.2373 | 0.62071 | 0.56695 |
| C28 | 0.45136 | 0.50836 | 0.27167 | C57 | 0.20225 | 0.59995 | 0.58412 |
| C29 | 0.4737 | 0.49345 | 0.32085 | C58 | 0.18643 | 0.56694 | 0.47801 |

Continuous (Table S2)

| Atom | x/a | y/b | z/c | Atom | x/a | y/b | z/c |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C59 | 0.15043 | 0.54272 | 0.54611 | O94 | 0.55116 | 0.04217 | 1.12888 |
| C60 | 0.06628 | 0.50066 | 0.51526 | O95 | 0.03054 | 0.53167 | 0.8047 |
| C61 | 0.01017 | 0.45985 | 0.31285 | O96 | 0.42899 | 0.43868 | 0.171 |
| C62 | 0.02951 | 0.48861 | 0.48527 | O97 | 0.5616 | 0.52172 | 0.52563 |
| C63 | 0.01257 | 0.50192 | 0.64602 | O98 | 0.48433 | 0.03746 | 0.53628 |
| C64 | 0.58939 | 0.13348 | 0.72852 | O99 | 0.43866 | 0.91378 | 0.14689 |
| C65 | 0.54364 | 0.04903 | 0.89174 | O100 | 0.51578 | 0.93492 | 0.64883 |
| C66 | 0.52993 | -0.00736 | 0.71674 | H101 | 0.90904 | 0.42221 | 0.75111 |
| C67 | 0.52255 | 0.01895 | 0.7001 | H102 | 0.9588 | 0.41405 | 0.14448 |
| C68 | 0.49296 | 0.01246 | 0.55459 | H103 | 0.65146 | 0.18419 | 0.79835 |
| C69 | 0.41183 | 0.83225 | 0.62778 | H104 | 0.67461 | 0.24256 | 0.67369 |
| C70 | 0.45369 | 0.91791 | 0.37901 | H105 | 0.58451 | 0.21903 | 0.19805 |
| C71 | 0.47773 | 0.9531 | 0.48059 | H106 | 0.56043 | 0.15948 | 0.33756 |
| C72 | 0.5079 | 0.96027 | 0.61426 | H107 | 0.69703 | 0.28362 | 0.31656 |
| C73 | 0.47116 | 0.97982 | 0.4405 | H108 | 0.68601 | 0.37053 | 0.30609 |
| C74 | 0.84161 | 0.41458 | 0.16635 | H109 | 0.59939 | 0.27263 | 0.4097 |
| C75 | 0.92055 | 0.43616 | 0.51981 | H110 | 0.74614 | 0.32445 | 0.59198 |
| C76 | 0.95789 | 0.45566 | 0.48071 | H111 | 0.80705 | 0.36 | 0.53742 |
| C77 | 0.9751 | 0.44328 | 0.3108 | H112 | 0.792 | 0.4197 | -0.10777 |
| C78 | 0.97717 | 0.48524 | 0.64455 | H113 | 0.73131 | 0.38453 | -0.05292 |
| N79 | 0.4328 | 0.54845 | 0.3887 | H114 | 0.64543 | 0.37968 | 0.06852 |
| N80 | 0.45352 | 0.53428 | 0.44079 | H115 | 0.61017 | 0.40549 | 0.12673 |
| N81 | 0.55825 | 0.41109 | 0.36125 | H116 | 0.5492 | 0.32924 | 0.75627 |
| N82 | 0.5358 | 0.42335 | 0.40717 | H117 | 0.58452 | 0.30425 | 0.70698 |
| N83 | 0.1262 | 0.55042 | 0.52049 | H118 | 0.45268 | 0.58221 | 0.73097 |
| N84 | 0.0927 | 0.52953 | 0.6487 | H119 | 0.53272 | 0.37037 | 0.63409 |
| N85 | 0.56254 | 0.10523 | 0.65474 | H120 | 0.46983 | 0.54245 | 0.6207 |
| N86 | 0.54717 | 0.08052 | 0.87915 | H121 | 0.5142 | 0.40946 | 0.53338 |
| N87 | 0.42914 | 0.85674 | 0.44291 | H122 | 0.47512 | 0.42105 | 0.19282 |
| N88 | 0.44784 | 0.89038 | 0.54431 | H123 | 0.51697 | 0.53908 | 0.47151 |
| N89 | 0.86352 | 0.41531 | 0.35348 | H124 | 0.34458 | 0.5801 | 0.14152 |
| N90 | 0.89872 | 0.43529 | 0.31457 | H125 | 0.37926 | 0.55335 | 0.18661 |
| N91 | 0.43148 | 0.49789 | 0.06753 | H126 | 0.44147 | 0.62788 | 0.82297 |
| O92 | 0.56789 | 0.47115 | 0.16181 | H127 | 0.40742 | 0.65453 | 0.7785 |
| O93 | 0.07811 | 0.51141 | 0.76167 | H128 | 0.40253 | 0.73711 | 0.1519 |

Continuous (Table S2)

| Atom | x/a | y/b | z/c | Atom | x/a | y/b | z/c |
| --- | --- | --- | --- | --- | --- | --- | --- |
| H129 | 0.42937 | 0.79829 | 0.22056 | H143 | 0.5549 | 0.09004 | 1.09248 |
| H130 | 0.35479 | 0.78315 | 0.86767 | H144 | 0.55265 | -0.00281 | 0.82681 |
| H131 | 0.32789 | 0.72271 | 0.79647 | H145 | 0.01616 | 0.53844 | 0.92055 |
| H132 | 0.30524 | 0.5897 | 0.44415 | H146 | 0.42304 | 0.41522 | 0.11419 |
| H133 | 0.39339 | 0.68685 | 0.4464 | H147 | 0.57586 | 0.51118 | 0.5624 |
| H134 | 0.29659 | 0.67843 | 0.42586 | H148 | 0.46269 | 0.0298 | 0.42389 |
| H135 | 0.19516 | 0.53031 | 0.26262 | H149 | 0.40929 | 0.83837 | 0.85458 |
| H136 | 0.25547 | 0.56697 | 0.20857 | H150 | 0.45842 | 0.89514 | 0.75488 |
| H137 | 0.24835 | 0.64516 | 0.6676 | H151 | 0.44842 | 0.97464 | 0.32881 |
| H138 | 0.18766 | 0.60907 | 0.69633 | H152 | 0.53849 | 0.94318 | 0.74377 |
| H139 | 0.14444 | 0.51884 | 0.64124 | H153 | 0.8503 | 0.43044 | -0.02783 |
| H140 | 0.10755 | 0.55107 | 0.50868 | H154 | 0.90968 | 0.44937 | 0.12957 |
| H141 | 0.02228 | 0.44895 | 0.18691 | H155 | 0.96457 | 0.49485 | 0.77931 |
| H142 | 0.60098 | 0.13456 | 0.93938 | H156 | 0.93344 | 0.40241 | 0.14459 |

Fig. S9. SEM images (a, b) and TEM images (c, d) of DHTP–TPB COF.

Fig. S10. Photograph images of Pb2+ solution with a) Ci=250 ppm and b) Ci=500 ppm at pH 4.0, and c) Ci=250 ppm and d) Ci=500 ppm at pH 6.0.

Fig. S11. Langmuir isotherm model.

Fig. S12. Freundlich isotherm model.

Fig. S13. Pseudo-first order model.

Fig. S14. Pseudo-second order model.

Fig. S15. Plot of lnKd versus 1/T for adsorption of Pb2+ onto DHTP–TPB COF

Figure S16. XPS spectra of DHTP–TPB COF before and after Pb2+ adsorption.

Figure S17. Coordination of Pb2+ with the hydroxyl groups in COFs structure.

Table S3. The adsorption capacity of different adsorbents for Pb2+.

| Materials | pH | Capacity (mg/g) | References |
| --- | --- | --- | --- |
| DHTP–TPB COF | 4.0 ± 0.1 6.0 | 154.3 419.6 | This work |
| COF-TP COF-TE | 6.5 6.5 | 140.0 185.7 | Chem. Eng. J. 2019, 370, 822–830 |
| COF-SH | 5.0-6.0 | 239.0 | Colloids and Surfaces A 2020, 600, 125004 |
| COOH@COF | 6.0 | 123.9 | Ind. Eng. Chem. Res. 2019, 58, 17660−17667 |
| Co-Fe2O3 Ni-Fe2O3 Fe2O3 | 5.0 | 136.0 97.5 93.9 | J. Cleaner Production 2019, 211 1250-1258 |
| MIL-101 Fe-MIL-101 | 6.0 | 57.96 86.20 | J. Environ. Chem. Eng. 2018, 6 4093–4102 |
| FFO@Sil@Chi-DTPA | 6.0 | 111.7 | J. Hazard. Mater. 2022 422, 126856 |
| Co0.6Fe2.4O4 | 6.0 | 80.32 | Colloids and Surfaces A 2015, 469, 211–223 |
| Mg2Al LDH | 5.7 | 57.51 | Chem. Eng. J. 2011,171, 167–174 |
| ES-PAN/AHCNs | 6.0 | 192 | Colloids Surfaces A 2021, 627, 127177 |
| UiO-66-1:1-120 UiO-66-1:2-50 | 6.0 | 125.1 149.8 | Langmuir 2021, 37, 13602−13609 |
| MIL-101(Fe)/GO | 6.0 | 128.6 | New J. Chem. 2019, 43, 1032--1037 |