Supplementary Material

Cellulose Based Cation-Exchange Fiber as Filtration Material for the Rapid Removal of Methylene Blue from Wastewater

Xinyi Shaoa, Jian Wanga, b, *, Zetan Liua, Na Hua, Min Liua, Chao Duana, Ruimin Zhanga, Cailin Quana

a: College of Bioresources Chemical and Materials Engineering, Shaanxi University of Science & Technology, Xi’an 710021, China

b: National Demonstration Center for Experimental Light Chemistry Engineering Education, Shaanxi University of Science & Technology, Xi’an 710021, China

*Corresponding author: Tel: +86-18229003848

E-mail: zzwangjian@sust.edu.cn

DS=nn+100-n×242162                                                  (S1)

Where DS is the degree of substitution; n is the content of the carboxyl group (mol per 100g sample); 242 is the relative molecular mass of carboxymethyl cellulose; 162 is the relative molecular mass of cellulose.

Table S1 The model dyes used by each cationic dye bio-adsorbent.

| Samples | Model dye | Reference |
| --- | --- | --- |
| Hemicellulose hydrogel | Methylene blue | Sun et al. (2015) |
| Soy Protein | Methylene blue | Liu et al. (2016) |
| Lignin sulfonate polymer | Malachite green | Tang et al. (2014) |
| Cotton gin trash | Methylene blue | Haque et al. (2020) |
| Magnetic chitosan | Methylene blue | Chen et al. (2020) |
| Oxidized chitosan | Methylene blue | Leon et al. (2018) |
| Sulfonated cellulose | Crystal violet | Zhou et al. (2014) |
| Phosphated cellulose | Rhodamine B | Silva et al. (2020) |
| CMC aerogel | Rhodamine B | Xiang et al. (2018) |
| CMC hydrogel | Methylene blue | Dai et al. (2017) |
| CMC membrane | Methylene blue | Sabarish et al. (2018) |
| CMC aerogel globules | Methylene blue | Huang et al. (2019) |
| CMC microbeads | Methylene blue | Eltaweil et al. (2020) |
| CMC nano-adsorbent | Methyl violet | Sharma et al. (2020) |
| CEF | Methylene blue | This work |

Considering that one anion is combined with one cation, and the molecular weight of MB is 319.85, the theoretical adsorption capacity can be calculated by the equation given below:

qse=Cc×MM                                                   (S2)

Where qse is the theoretical adsorption capacity (i.e., saturated electrostatic adsorption capacity) (mg·g-1); Cc is the content of the carboxyl group (mmol per 100g sample); MM is the relative molecular mass of MB.

References

Chen B, Long F, Chen S, Cao Y, Pan X (2020) Magnetic chitosan biopolymer as a versatile adsorbent for simultaneous and synergistic removal of different sorts of dyestuffs from simulated wastewater. Chem Eng Technol 385: 123926. https:// doi.org/ 10.1016/j.cej.2019.123926

Dai H, Huang Y, Huang H (2017) Eco-friendly polyvinyl alcohol/carboxymethyl cellulose hydrogels reinforced with graphene oxide and bentonite for enhanced adsorption of methylene blue. Carbohydr Polym 185: 1-11. https://doi.org/10.1016/j.carbpol.2017.12.073

Eltaweil AS, Elgarhy GS, El-Subruiti GM, Omer AM (2020) Novel carboxymethyl cellulose/carboxylated graphene oxide composite microbeads for efficient adsorption of cationic methylene blue dye. Int J Biol Macromol 154: 307-318. https://doi.org/10.1016/j.ijbiomac.2020.03.122.

Haque ANMA, Remadevi R, Rojas OJ, Wang X, Naebe M (2020) Kinetics and equilibrium adsorption of methylene blue onto cotton gin trash bioadsorbents. Cellulose 27: 6485-6504. https:// doi.org/ 10.1007/s10570-020-03238-y

Leon O, Alexandra MB, Soto D, Perez D, Rangel M (2018) Removal of anionic and cationic dyes with bioadsorbent oxidized chitosans. Carbohydr Polym 194: 375-383. https:// doi.org/ 10.1016/j.carbpol.2018.04.072

Liu F, Zou H, Hu J, Liu H, Huo Y (2016a) Fast removal of methylene blue from aqueous solution using porous soy protein isolate based composite beads. Chem Eng Technol 287: 410-418. https:// doi.org/ 10.1016/j.cej.2015.11.041

Sabarish R, Unnikrishnan G (2018) Polyvinyl alcohol/carboxymethyl cellulose/ZSM-5 zeolite biocomposite membranes for dye adsorption applications. Carbohydr Polym 199: 129-140. https://doi.org/10.1016/j.carbpol.2018.06.123.

Sharma G, Kumar A, Sharma S, Naushad M, Stadler FJ (2020) Carboxymethyl cellulose structured nano-adsorbent for removal of methyl violet from aqueous solution: isotherm and kinetic analyses. Cellulose, 27, 3677-3691. https://doi.org/10.1007/s10570-020-02989-y.

Silva MS, Silva LS, Ferreira FJL, Bezerra RDS, Marques TMF, Meneguin AB, Barud HS, Osajima JA, Silva Filho EC (2020) Study of interactions between organic contaminants and a new phosphated biopolymer derived from cellulose. Int J Biol Macromol 146: 668-677. https://doi.org/10.1016/j.ijbiomac.2019.12.121.

Sun X, Gan Z, Jing Z, Wang H, Jin Y (2015) Adsorption of methylene blue on hemicellulose‐based stimuli‐responsive porous hydrogel. J Appl Polym Sci 132: 41606. https:// doi.org/ 10.1002/app.41606

Tang Y, Hu T, Zeng Y, Zhou Q, Peng Y (2014) Effective adsorption of cationic dyes by lignin sulfonate polymer based on simple emulsion polymerization: isotherm and kinetic studies. Rsc Adv 5: 3757-3766. https:// doi.org/ 10.1039/C4RA12229A

Xiang C, Wang C, Guo RH, Lan JW, Lin SJ, Jiang SX, Lai XX, Zhang Y, Xiao HY (2018) Synthesis of carboxymethyl cellulose-reduced graphene oxide aerogel for efficient removal of organic liquids and dyes. J Mater Sci 54: 1872-1883. https://doi.org/10.1007/s10853-018-2900-5.

Zhou Y, Zhang M, Wang X, Huang Q, Min Y, Ma T, Niu J (2014) Removal of Crystal Violet by a Novel Cellulose-Based Adsorbent: Comparison with Native Cellulose. Ind Eng Chem Res 53:5498-5506. https://doi.org/10.1021/ie404135y