Design and synthesis of Brønsted-Lewis acidic tetraimidazolyl ionic liquids for efficient catalytic conversion of glucose to 5-hydroxymethylfurfural in water/1-octanol

Jian Zhao, Chao Li, Xiaodong Fan, Hao Liu, Ziqi Liu, Jingchao Zhang, Zhizhong Sun* and Wenyi Chu*

School of Chemistry and Materials Science, Heilongjiang University, Harbin 150080, P. R. China.

Tel: +86-451-86609135

Fax: +86-451-86609135

E-mail: sunzz@hlju.edu.cn; wenyichu@hlju.edu.cn

Contents of Supporting Information

1. Characterization of the data................................................................ S2

2. NMR spectra………………………………………………………... S7

1. Characterization of the data

Tetrakis(bromomethyl)methane

m.p. 158 ~ 160 °C; 1H NMR (400 MHz, CDCl3) δ 3.59 (s, 8H); (Figure S1) 13C NMR (101 MHz, CDCl3) δ 43.2, 34.4; (Figure S2) FT-IR (KBr disc): v= 2953, 1421, 1269, 1187, 831, 612 cm-1; HRMS (ESI): m/z calcd for C5H8Br4+H+: 384.7438; found: 384.7439; elemental analysis calcd (%) for C5H8Br4: C 15.49, H 2.08, Br 82.43; found: C 15.47, H 2.09, Br 82.44.

Tetrakis(imidazol-1-ylmethyl)methane

m.p. 156 ~ 158 °C; 1H NMR (400 MHz, D2O) δ 7.40(s, 4H), 6.99 (s, 4H), 6.94 (s, 4H), 4.16(s, 8H); (Figure S3) 13C NMR (101 MHz, D2O) δ 139.1, 128.5, 121.5, 49.5, 42.3; (Figure S4) FT-IR (KBr disc): v= 1583, 1560, 1507, 1453, 1248, 1083, 1022, 915, 837, 742, 658, 623 cm-1; HRMS (ESI): m/z calcd for C17H20N8+H+: 337.1889; found: 337.1886; elemental analysis calcd (%) for C17H20N8: C 60.70, H 5.99, N 33.31; found: C 60.68, H 5.98, N 33.34.

Tetracation propanesulfonic acid type ionic liquid onium salt (Teim-PS)

m.p. 160 ~ 162 °C; 1H NMR (400 MHz, D2O) δ 9.04 (s, 4H), 7.71 (s, 4H), 7.64 (s, 4H), 4.60 (s, 8H), 4.46 (t, J =6.9 Hz, 8H), 2.98 (t, J = 7.2 Hz, 8H), 2.39 (m, 8H); (Figure S5) 13C NMR (101 MHz, D2O) δ 137.5, 124.4, 122.9, 51.1, 48.3, 47.3, 43.0, 24.9; (Figure S6) FT-IR (KBr disc): v= 3103, 1683, 1650, 1557, 1509, 1452, 1178, 1038, 882, 792, 690 cm-1; HRMS (ESI): m/z calcd for C29H44N8O12S4+H+: 825.2040; found: 825.2045; elemental analysis calcd (%) for C29H44N8O12S4: C 42.22, H 5.38, N 13.58, S 15.55; found: C 42.24, H 5.36, N 13.57, S 15.57.

Tetracation propanesulfonic acid type ionic liquid chloride ([TeimILs]Cl4)

m.p. 96 ~ 98 °C; 1H NMR (400 MHz, D2O) δ 8.78 (s, 4H), 7.73 (s, 4H), 7.61 (s, 4H), 4.43 (t, J = 6.7 Hz, 8H), 4.04 (t, J = 6.3 Hz, 8H), 2.99 (t, J = 6.8 Hz, 8H), 2.35 (m, 8H); (Figure S7) 13C NMR (101 MHz, D2O) δ 136.7, 122.5, 121.1, 54.1, 49.6, 47.7, 43.0, 25.5; (Figure S8) FT-IR (KBr disc): v= 3107, 2960, 2918, 1685, 1597, 1454, 1286, 1244, 835, 796, 634 cm-1; HRMS (ESI): m/z calcd for [C29H48Cl4N8O12S4-4Cl]/4: 207.0563; found: 207.0561; elemental analysis calcd (%) for C29H48Cl4N8O12S4: C 35.88, H 4.98, Cl 14.61, N 11.54, S 13.21; found: C 35.86, H 4.99, Cl 14.63, N 11.53, S 13.22.

Tetracation propanesulfonic acid type ionic liquid aluminum salt ([Teim-PS][AlCl4]4)

m.p. 102 ~ 104 °C; 1H NMR (400 MHz, D2O) δ 8.76 (s, 4H), 7.38 (d, J= 10.5 Hz, 8H), 4.33 (s, 8H), 4.16 (s, 8H), 2.69 (t, J = 5.9 Hz, 8H), 2.12 - 2.04 (m, 8H); (Figure S9) 13C NMR (101 MHz, D2O) δ 137.7, 124.6, 122.4, 51.3, 48.5, 46.9, 42.3, 24.7; (Figure S10) FT-IR (KBr disc): v= 3041, 1656, 1606, 1448, 1300, 1263, 1178, 952, 810, 702, 605 cm-1; HRMS (ESI): m/z calcd for [C29H48Al4Cl16N8O12S4-4AlCl4]/4: 207.0563; found: 207.0562; elemental analysis calcd (%) for C29H48Al4Cl16N8O12S4: C 23.16, H 3.22, Cl 37.71, N 7.45, S 8.53; found: C 23.15, H 3.20, Cl 37.73, N 7.44, S 8.51.

Tetracation butanesulfonic acid type ionic liquid onium salt (Teim-ES)

m.p. 158 ~ 60 °C; 1H NMR (400 MHz, D2O) δ 8.76(s, 4H), 7.57 (s, 4H), 7.49 (s, 4H), 4.43 (t, J = 7.1 Hz, 8H), 3.01 - 2.88 (m, 8H), 2.42 - 2.28 (m, 8H); (Figure S11) 13C NMR (101 MHz, D2O) δ 134.6, 121.7, 120.2, 58.5, 49.2, 47.3, 43.1; (Figure S12) FT-IR (KBr disc): v= 3089, 1670, 1601, 1508, 1458, 1240, 1055, 885, 742, 617 cm-1; HRMS (ESI): m/z calcd for C25H36N8O16S4+H+: 833.1210; found: 833.1214; elemental analysis calcd (%) for C25H36N8O16S4: C 36.05, H 4.36, N 13.45, S 15.40; found: C 36.03, H 4.35, N 13.46, S 15.42.

Tetracation butanesulfonic acid type ionic liquid chloride ([Teim-ES]Cl4)

m.p. 94 ~ 96 °C; 1H NMR (400 MHz, D2O) δ 7.67 (s, 4H), 7.08 (d, J = 16.1 Hz, 8H), 4.15 (s, 8H), 3.15 (t, J = 6.9 Hz, 8H), 2.33 (t, J = 7.6 Hz, 8H); (Figure S13) 13C NMR (101 MHz, D2O) δ 138.9, 127.4, 121.8, 59.4, 48.7, 47.8, 42.6; (Figure S14) FT-IR (KBr disc): v= 3059, 1664, 1592, 1435, 1315, 1249, 1089, 939, 852, 758 cm-1; HRMS (ESI): m/z calcd for [C25H40Cl4N8O16S4-4Cl]/4: 209.0356; found: 209.0358; elemental analysis calcd (%) for C25H40Cl4N8O16S4: C 30.68, H 4.12, Cl 14.49, N 11.45, S 13.10; found: C 30.66, H 4.12, Cl 14.48, N 11.47, S 13.12.

Tetracation butanesulfonic acid type ionic liquid aluminum salt ([Teim-ES][AlCl4]4)

m.p. 98 ~ 100 °C; 1H NMR (400 MHz, D2O) δ 7.61 (s, 4H), 7.10 (s, 4H), 7.05 (s, 4H), 4.14 (s, 8H), 3.18 (t, J = 6.4 Hz, 8H), 2.09 (t, J = 6.4 Hz, 8H); (Figure S15) 13C NMR (101 MHz, D2O) δ 137.1, 121.7, 120.2, 57.9, 49.0, 47.3, 41.9; (Figure S16) FT-IR (KBr disc): v= 3035, 1666, 1602, 1429, 1303, 1242, 1157, 933, 848, 771 cm-1; HRMS (ESI): m/z calcd for [C25H40Al4Cl16N8O16S4-4AlCl4]/4: 209.0356; found: 209.0351; elemental analysis calcd (%) for C25H40Al4Cl16N8O16S4: C 19.86, H 2.67, Cl 37.51, N 7.41, S 8.48; found: C 19.85, H 2.65, Cl 37.53, N 7.38, S 8.49.

Tetracation butanesulfonic acid type ionic liquid onium salt (Teim-BS)

m.p. 165 ~ 167 °C; 1H NMR (400 MHz, D2O) δ 8.88 (s, 4H), 7.60 (s, 4H), 7.51 (s, 4H), 4.40 (t, J = 7.0 Hz, 8H), 4.28 (t, J = 6.5 Hz, 8H), 3.15 (t, J = 6.4 Hz, 8H), 2.91 (t, J = 7.3 Hz, 8H), 2.32 (dd, J = 7.1 Hz, 8H); (Figure S17) 13C NMR (101 MHz, D2O) δ 137.5, 124.4, 122.9, 51.0, 48.2, 47.2, 42.9, 24.9; (Figure S18) FT-IR (KBr disc): v= 3062, 1651, 1433, 1321, 1215, 1143, 1012, 861, 735 cm-1; HRMS (ESI): m/z calcd for C33H52N8O12S4+H+: 881.2666; found: 881.2669; elemental analysis calcd (%) for C33H52N8O12S4: C 44.99, H 5.95, N 12.72, S 14.56; found: C 44.98, H 5.97, N 12.74, S 14.53.

Tetracation butanesulfonic acid type ionic liquid chloride ([Teim-BS]Cl4)

m.p. 103 ~ 105 °C; 1H NMR (400 MHz, D2O) δ 7.95 (s, 4H), 7.62 (s, 4H), 7.14 (s, 4H), 4.19 (s, 8H), 4.02 (s, 8H), 3.05 (s, 8H), 2.35 (s, 8H); (Figure S19) 13C NMR (101 MHz, D2O) δ 137.4, 124.5, 122.9, 50.9, 48.3, 47.2, 42.9, 24.8; (Figure S20) FT-IR (KBr disc): v= 3047, 1662, 1597, 1442, 1302, 1212, 1085, 844, 731 cm-1; HRMS (ESI): m/z calcd for [C33H56Cl4N8O12S4-4Cl]/4: 221.0720; found: 221.0724; elemental analysis calcd (%) for C33H56Cl4N8O12S4: C 38.60, H 5.50, Cl 13.81, N 10.91, S 12.49; found: C 38.63, H 5.48, Cl 13.82, N 10.93, S 12.48.

Tetracation butanesulfonic acid type ionic liquid aluminum salt ([Teim-BS][AlCl4]4)

m.p. 106 ~ 108 °C; 1H NMR (400 MHz,   D2O) δ 8.87 (s, 4H), 7.59 (s, 4H), 7.49 (s, 4H), 4.39 (t, J = 7.2 Hz, 8H), 4.27 (t, J = 6.6 Hz, 8H), 3.13(t, J = 6.6 Hz, 8H), 2.90 (t, J = 7.2 Hz, 8H), 2.36 – 2.28 (m, 8H); (Figure S21) 13C NMR (101 MHz, D2O) δ 137.4, 124.5, 123.1, 50.9, 48.4, 47.0, 42.9, 24.9; (Figure S22) FT-IR (KBr disc): v= 3068, 1670, 1560, 1458, 1419, 1188, 900, 794, 671 cm-1; HRMS (ESI): m/z calcd for [C33H56Al4Cl16N8O12S4-4AlCl4]/4: 221.0720; found: 221.0722; elemental analysis calcd (%) for C33H56Al4Cl16N8O12S4: C 25.40, H 3.62, Cl 36.35, N 7.18, S 8.22; found: C 25.36, H 3.63, Cl 36.36, N 7.19, S 8.20.

Tetracationic benzenesulfonic acid type ionic liquid onium salt (Teim-BD)

m.p. 169 ~ 171 °C; 1H NMR (400 MHz, D2O) δ 8.76 (s, 4H), 7.61 (dd, J = 17.0, 10.4 Hz, 4H), 7.50 (t, J = 1.7 Hz, 4H), 7.44 (d, J = 3.3 Hz, 4H), 7.37 – 7.17 (m, 12H), 5.98 (d, J = 6.1 Hz, 8H), 4.31 (t, J = 7.1 Hz, 8H); (Figure S23) 13C NMR (101 MHz, D2O) δ 135.7, 130.3, 125.3, 124.7, 123.6, 122.7, 122.5, 121.3, 51.6, 47.3, 41.7; (Figure S24) FT-IR (KBr disc): v= 3025, 1681, 1562, 1482, 1312, 1241, 966, 893, 715, 692 cm-1; HRMS (ESI): m/z calcd for C45H44N8O12S4+H+: 1017.2040; found: 1017.2036; elemental analysis calcd (%) for C45H44N8O12S4: C 53.14, H 4.36, N 11.02, S 12.61; found: C 53.16, H 4.35, N 11.00, S 12.64.

Tetracationic benzenesulfonic acid type ionic liquid chloride ([Teim-BD]Cl4)

m.p. 109 ~ 111 °C; 1H NMR (400 MHz, D2O) 7.49 (s, 4H), 7.22 (dd, J = 17.0, 10.3 Hz, 4H), 7.08 (s, 4H), 6.98 (s, 4H), 6.97 – 6.81 (m, 12H), 5.50 (s, 8H), 4.56 (d, J = 5.7 Hz, 8H); (Figure S25) 13C NMR (101 MHz, D2O) δ 135.8, 130.5, 125.3, 124.7, 123.7, 122.7, 122.4, 121.3, 51.6, 47.7, 41.9; (Figure S26) FT-IR (KBr disc): v= 3070, 1658, 1597, 1431, 1310, 1210, 1136, 1018, 856, 763 cm-1; HRMS [C45H48Cl4N8O12S4-4Cl]/4: 255.0563; found: 255.0565; elemental analysis calcd (%) for C45H48Cl4N8O12S4: C 46.48, H 4.16, Cl 12.19, N 9.64, S 11.03; found: C 46.45, H 4.17, Cl 12.21, N 9.61, S 11.05.

Tetracationic benzenesulfonic acid type ionic liquid aluminum salt ([Teim-BD][AlCl4]4)

m.p. 114 ~ 116 °C; 1H NMR (400 MHz, D2O) δ 8.86 (s, 4H), 7.67 – 7.61 (m, 4H), 7.57 – 7.55 (m, 4H), 7.50 (t, J = 1.8 Hz, 4H), 7.43 – 7.30 (m, 12H), 5.42 (s, 8H), 4.35 (t, J = 7.1 Hz, 8H); (Figure S27) 13C NMR (101 MHz, D2O) δ 137.5, 130.0, 124.4, 123.6, 122.9, 122.5, 122.3, 121.3, 51.0, 47.2, 42.9; (Figure S28) FT-IR (KBr disc): v= 3057, 1676, 1592, 1458, 1300, 1220, 1091, 855, 729 cm-1; HRMS (ESI): m/z calcd for [C45H48Al4Cl16N8O12S4-4AlCl4]/4: 255.0563; found: 255.0567; elemental analysis calcd (%) for C45H48Al4Cl16N8O12S4: C 31.86, H 2.85, Cl 33.44, N 6.61, S 7.56; found: C 31.86, H 2.83, Cl 33.42, N 6.62, S 7.57.

2. NMR spectra

Figure S1. 1H NMR of tetrakis(bromomethyl)methane

Figure S2. 13C NMR of tetrakis(bromomethyl)methane

Figure S3. 1H NMR of tetrakis(imidazol-1-ylmethyl)methane

Figure S4. 13C NMR of tetrakis(imidazol-1-ylmethyl)methane

Figure S5. 1H NMR of Teim-PS

Figure S6. 13C NMR of Teim-PS

Figure S7. 1H NMR of [Teim-PS]Cl4

Figure S8. 13C NMR of [Teim-PS]Cl4

Figure S9. 1H NMR of [Teim-PS][AlCl4]4

Figure S10. 13C NMR of [Teim-PS][AlCl4]4

Figure S11. 1H NMR of Teim-ES

Figure S12. 13C NMR of Teim-ES

Figure S13. 1H NMR of [Teim-ES]Cl4

Figure S14. 13C NMR of [Teim-ES]Cl4

Figure S15. 1H NMR of [Teim-ES][AlCl4]4

Figure S16. 13C NMR of [Teim-ES][AlCl4]4

Figure S17. 1H NMR of Teim-BS

Figure S18. 13C NMR of Teim-BS

Figure S19. 1H NMR of [Teim-BS]Cl4

Figure S20. 13C NMR of [Teim-BS]Cl4

Figure S21. 1H NMR of [Teim-BS][AlCl4]4

Figure S22. 13C NMR of [Teim-BS][AlCl4]4

Figure S23. 1H NMR of Teim-BD

Figure S24. 13C NMR of Teim-BD

Figure S25. 1H NMR of [Teim-BD]Cl4

Figure S26. 13C NMR of [Teim-BD]Cl4

Figure S27. 1H NMR of [Teim-BD][AlCl4]4

Figure S28. 13C NMR of [Teim-BD][AlCl4]4