Supporting Information

Preparation of Simulated Naturally-derived Nanoplastics as Standard Substance

Zhongtang Wanga,‡, Xianlei Gaob,‡, Xin Lua, Hongyan Zhanga,* and Zhenzhen Jiaa,*

a Shandong Provincial Key Laboratory of Animal Resistance Biology, Key Laboratory of Food Nutrition and Safety of Shandong Normal University, College of Life Science, Shandong Normal University, Jinan, 250014, PR China.

b Department of Orthopedic Surgery, Qilu Hospital, Cheeloo College of Medicine, Shandong University, Jinan, Shandong 250012, China.

*E-mail: zhanghongyan@sdnu.edu.cn; jiazhenzhen@sdnu.edu.cn.

Figure S1, S2, S3 and S4 show the schematic diagram of how the mortar is selected, the schematic diagram of how the basic grinding time is determined, the diagram of transmission electron microscope (TEM) characterization for gold and silver nanoparticles, and the schematic diagram of particle parameters as measured using the Image proplus 6.0 software, respectively. All raw data can be found as Table S1~6 .

Figure S1. Schematic diagram of mortar selection. a, b) Particles produced in the glass mortar during grinding. c, d) Particles produced in an agate mortar during grinding.

Figure S2. Image of the change occurring to plastic particles in the process of grinding. a~d) The corresponding grinding time is 0 min, 10 min, 20 min and 30 min, respectively.

Figure S3. TEM characterization of gold and silver nanoparticles. a) Gold nanoparticles with a particle size of 40 nm. b) Silver nanoparticles with a particle size of 20 nm.

Figure S4. Diagram of image processing by Image proplus 6.0 software processes image. a, e, h) Scanning electron microscope characteristic diagram of commercially available, self-made, and naturally-derived NPs. b~c, f~g, i~j) The software is used to select and measure the parameters of NPs.

Table S1. The number of NPs on the grinding conditions of different sample quality.

|  | 1 |  |  | 2 |  |  | 3 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 0.2g | 0.4g | 0.6g | 0.2g | 0.4g | 0.6g | 0.2g | 0.4g | 0.6g |
| 20 min | 5 | 11 | 25 | 4 | 12 | 45 | 6 | 16 | 53 |
|  | 6 | 15 | 43 | 8 | 15 | 35 | 3 | 14 | 45 |
|  | 8 | 9 | 46 | 11 | 25 | 36 | 2 | 11 | 49 |
|  | 9 | 16 | 37 | 3 | 13 | 40 | 9 | 10 | 36 |
|  | 8 | 17 | 32 | 7 | 19 | 41 | 8 | 14 | 29 |
| 40 min | 4 | 15 | 35 | 6 | 19 | 42 | 9 | 14 | 30 |
|  | 9 | 22 | 30 | 9 | 15 | 34 | 5 | 13 | 49 |
|  | 8 | 19 | 19 | 12 | 21 | 38 | 1 | 11 | 38 |
|  | 10 | 18 | 29 | 0 | 16 | 36 | 8 | 19 | 36 |
|  | 12 | 16 | 37 | 8 | 13 | 29 | 6 | 17 | 32 |
| 60 min | 8 | 12 | 16 | 7 | 19 | 31 | 6 | 21 | 43 |
|  | 1 | 16 | 39 | 3 | 21 | 36 | 8 | 13 | 53 |
|  | 6 | 8 | 46 | 8 | 23 | 35 | 2 | 26 | 46 |
|  | 12 | 16 | 48 | 6 | 21 | 50 | 9 | 10 | 38 |
|  | 7 | 18 | 42 | 9 | 15 | 48 | 11 | 18 | 34 |

Table S2. Dimension parameter of there kinds of NPs.

| Commercialized NP |  |  |  |  | Self-made NPs |  |  |  |  | Naturally-derived NPs |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Object | Area | Angle | Size (length) | Size (width) | Object | Area | Angle | Size (length) | Size (width) | Object | Area | Angle | Size (length) | Size (width) |
| 1 | 1708 | 128.4269 | 65.2738 | 33.45203 | 1 | 17585 | 82.24453 | 217.3941 | 186.4578 | 1 | 19026 | 36.73478 | 211.8909 | 180.4325 |
| 2 | 1323 | 27.60772 | 74.32281 | 26.30844 | 2 | 17366 | 27.06077 | 186.1384 | 186.061 | 2 | 3687 | 175.7596 | 84.10376 | 57.80521 |
| 3 | 1090 | 120.8743 | 59.16776 | 25.69424 | 3 | 16400 | 134.8484 | 200.769 | 160.6791 | 3 | 1813 | 89.92752 | 55.00751 | 48.01135 |
| 4 | 1068 | 90 | 37 | 35 | 4 | 13970 | 60.80544 | 174.5122 | 117.2835 | 4 | 1770 | 51.12323 | 67.97177 | 47.68233 |
| 5 | 1016 | 180 | 35.00006 | 35 | 5 | 7220 | 29.69102 | 135.4504 | 82.51981 | 5 | 1426 | 9.49547 | 60.17126 | 32.23199 |
| 6 | 1016 | 180 | 35 | 35 | 6 | 6273 | 113.963 | 103.4639 | 86.50756 | 6 | 1289 | 76.8485 | 65.34293 | 30.57831 |
| 7 | 1016 | 180 | 35 | 35 | 7 | 5232 | 126.5374 | 126.958 | 76.95386 | 7 | 1266 | 127.0528 | 63.25586 | 29.54495 |
| 8 | 1016 | 180 | 35 | 35 | 8 | 5231 | 142.616 | 100.0857 | 69.9523 | 8 | 1212 | 117.2407 | 47.81686 | 39.33096 |
| 9 | 1016 | 90 | 35 | 35 | 9 | 4490 | 83.92727 | 87.78128 | 69.75525 | 9 | 1175 | 179.2176 | 54.09052 | 31.90146 |
| 10 | 956 | 90 | 35 | 33 | 10 | 4206 | 130.3198 | 116.4319 | 66.86866 | 10 | 1146 | 125.4936 | 43.3587 | 33.94877 |
| 11 | 905 | 132.614 | 33.41129 | 32.85195 | 11 | 4017 | 102.8392 | 106.4246 | 47.04959 | 11 | 1134 | 133.7276 | 55.36055 | 28.27698 |
| 12 | 904 | 90 | 33 | 33 | 12 | 3872 | 122.2697 | 94.65283 | 68.75485 | 12 | 1086 | 176.3997 | 53.39777 | 27.70023 |
| 13 | 904 | 90 | 33 | 33 | 13 | 3859 | 160.3207 | 81.53949 | 68.06934 | 13 | 1068 | 74.6982 | 44.72424 | 39.46472 |
| 14 | 904 | 90 | 33 | 33 | 14 | 3123 | 52.42703 | 74.56863 | 64.021 | 14 | 1046 | 4.04107 | 46.22705 | 34.49014 |
| 15 | 854 | 1.82661 | 33.20636 | 31.20737 | 15 | 2979 | 178.9376 | 74.22833 | 60.15659 | 15 | 1040 | 117.6666 | 61.29134 | 22.61447 |
| 16 | 850 | 90 | 33 | 31 | 16 | 2917 | 78.62955 | 68.63689 | 61.77428 | 16 | 1031 | 101.2473 | 47.65765 | 31.7811 |
| 17 | 804 | 180 | 31 | 31 | 17 | 2581 | 160.9083 | 88.64755 | 74.69009 | 17 | 1012 | 66.29077 | 55.65302 | 26.50879 |
| 18 | 756 | 27.82318 | 42.57324 | 21.54422 | 18 | 2497 | 15.91475 | 68.81534 | 57.40659 | 18 | 990 | 129.0647 | 54.22849 | 28.71759 |
| 19 | 751 | 0.56423 | 31.06743 | 29.06752 | 19 | 2475 | 23.30879 | 64.85364 | 50.79453 | 19 | 915 | 61.56537 | 55.28436 | 29.31073 |
| 20 | 751 | 0.56423 | 31.06741 | 29.06754 | 20 | 2433 | 102.8152 | 77.38788 | 47.38191 | 20 | 909 | 27.19413 | 51.42648 | 28.30042 |
| 21 | 704 | 90 | 29 | 29 | 21 | 2260 | 153.4441 | 73.79276 | 49.64342 | 21 | 901 | 29.12935 | 39.13531 | 30.20001 |
| 22 | 602 | 154.9549 | 35.88318 | 19.33833 | 22 | 2064 | 29.59531 | 55.60815 | 52.72107 | 22 | 870 | 13.64577 | 54.54279 | 23.73816 |
| 23 | 568 | 90 | 27 | 25 | 23 | 2001 | 71.86674 | 67.32397 | 41.52016 | 23 | 841 | 88.59671 | 44.13373 | 30.89274 |
| 24 | 532 | 180 | 25 | 25 | 24 | 1985 | 149.6993 | 70.11243 | 54.06686 | 24 | 833 | 21.02803 | 50.83078 | 25.91959 |
| 25 | 378 | 90 | 21 | 21 | 25 | 1819 | 7.31762 | 57.07234 | 52.03988 | 25 | 802 | 173.4573 | 42.55606 | 29.49478 |
| 26 | 378 | 90 | 21 | 21 | 26 | 1728 | 145.0721 | 73.99494 | 50.72693 | 26 | 799 | 38.32611 | 34.57021 | 28.78735 |
| 27 | 378 | 90 | 21 | 21 | 27 | 1625 | 43.92063 | 65.38861 | 44.10026 | 27 | 782 | 16.7252 | 40.61481 | 25.67377 |
| 28 | 378 | 90 | 21 | 21 | 28 | 1599 | 16.3725 | 71.72582 | 33.53174 | 28 | 780 | 132.8259 | 36.90399 | 32.28891 |
| 29 | 378 | 90 | 21 | 21 | 29 | 1532 | 17.02202 | 55.65475 | 36.39412 | 29 | 777 | 164.0487 | 44.09251 | 24.72406 |
| 30 | 378 | 90 | 21 | 21 | 30 | 1465 | 128.0552 | 45.43579 | 39.71704 | 30 | 758 | 3.30989 | 42.21863 | 22.25198 |
| 31 | 378 | 90 | 21 | 21 | 31 | 1454 | 39.30696 | 49.39362 | 43.1312 | 31 | 752 | 173.3893 | 41.11554 | 22.08398 |
| 32 | 378 | 90 | 21 | 21 | 32 | 1436 | 173.9936 | 47.52719 | 46.21878 | 32 | 737 | 128.1111 | 41.1167 | 27.07666 |
| 33 | 378 | 90 | 21 | 21 | 33 | 1431 | 9.10801 | 48.54047 | 48.26935 | 33 | 731 | 158.3747 | 40.86987 | 25.48468 |
| 34 | 378 | 90 | 21 | 21 | 34 | 1410 | 52.78415 | 43.95087 | 41.34006 | 34 | 698 | 142.0686 | 37.70828 | 23.94031 |
| 35 | 378 | 90 | 21 | 21 | 35 | 1407 | 58.29538 | 45.71753 | 41.53911 | 35 | 686 | 47.83902 | 34.10962 | 25.70478 |
| 36 | 378 | 90 | 21 | 21 | 36 | 1406 | 87.22237 | 47.84668 | 40.63144 | 36 | 672 | 129.5318 | 35.36652 | 25.10779 |
| 37 | 378 | 90 | 21 | 21 | 37 | 1403 | 60.85293 | 45.26376 | 41.93848 | 37 | 654 | 128.4681 | 34.3643 | 25.33344 |
| 38 | 378 | 90 | 21 | 21 | 38 | 1401 | 45.7722 | 49.51202 | 38.18031 | 38 | 635 | 140.4146 | 40.96265 | 21.81586 |
| 39 | 378 | 90 | 21 | 21 | 39 | 1325 | 148.9243 | 47.49261 | 38.21295 | 39 | 631 | 125.7961 | 37.74707 | 24.50439 |
| 40 | 378 | 90 | 21 | 21 | 40 | 1324 | 18.15495 | 41.40527 | 41.15549 | 40 | 629 | 39.52555 | 35.36719 | 27.32538 |
| 41 | 378 | 90 | 21 | 21 | 41 | 1240 | 37.35847 | 71.12579 | 24.08392 | 41 | 610 | 18.26983 | 35.09839 | 23.70331 |
| 42 | 378 | 90 | 21 | 21 | 42 | 1196 | 175.2604 | 47.08212 | 34.46213 | 42 | 607 | 53.73219 | 38.00842 | 24.0827 |
| 43 | 378 | 90 | 21 | 21 | 43 | 1193 | 151.9683 | 54.11801 | 33.75896 | 43 | 602 | 5.85007 | 31.55203 | 24.38464 |
| 44 | 378 | 90 | 21 | 21 | 44 | 1173 | 82.03367 | 45.57629 | 44.14996 | 44 | 592 | 119.2746 | 30.29196 | 26.20813 |
| 45 | 378 | 90 | 21 | 21 | 45 | 1161 | 64.03983 | 59.08084 | 38.12906 | 45 | 591 | 121.1572 | 34.7868 | 22.92625 |
| 46 | 378 | 90 | 21 | 21 | 46 | 1088 | 174.5741 | 53.80267 | 39.15356 | 46 | 574 | 106.9895 | 31.90491 | 22.79306 |
| 47 | 378 | 90 | 21 | 21 | 47 | 1036 | 42.14469 | 42.05499 | 32.59045 | 47 | 569 | 170.2384 | 29.42792 | 25.68712 |
| 48 | 344 | 180 | 21 | 19 | 48 | 1021 | 23.79506 | 39.36648 | 39.17914 | 48 | 545 | 178.6326 | 36.03748 | 17.85168 |
| 49 | 344 | 180 | 21 | 19 | 49 | 1015 | 70.75026 | 40.82074 | 36.99945 | 49 | 534 | 90.38853 | 27.01971 | 24.01302 |
| 50 | 344 | 90 | 21 | 19 | 50 | 1011 | 140.8504 | 47.97699 | 41.80762 | 50 | 532 | 47.80051 | 30.54202 | 24.96103 |
| 51 | 344 | 180 | 21 | 19 | 51 | 919 | 95.05094 | 47.16965 | 37.12048 | 51 | 532 | 133.3025 | 34.77965 | 20.64371 |
| 52 | 344 | 180 | 21 | 19 | 52 | 918 | 51.90938 | 43.30914 | 31.63086 | 52 | 521 | 170.071 | 31.2254 | 22.06491 |
| 53 | 344 | 180 | 21 | 19 | 53 | 909 | 43.94479 | 39.66937 | 34.75952 | 53 | 495 | 113.0707 | 31.12744 | 22.06354 |
| 54 | 344 | 90 | 21 | 19 | 54 | 905 | 52.11748 | 49.11459 | 27.19019 | 54 | 477 | 149.5027 | 28.84711 | 20.73808 |
| 55 | 344 | 180 | 21 | 19 | 55 | 900 | 19.88452 | 36.05444 | 33.49344 | 55 | 474 | 28.17586 | 28.77379 | 23.01257 |
| 56 | 344 | 180 | 21 | 19 | 56 | 884 | 178.506 | 48.85297 | 37.83066 | 56 | 470 | 58.52135 | 27.77856 | 22.99219 |
| 57 | 344 | 90 | 21 | 19 | 57 | 874 | 90.69621 | 47.00867 | 25.96164 | 57 | 467 | 121.0042 | 30.01188 | 21.60541 |
| 58 | 344 | 90 | 21 | 19 | 58 | 872 | 92.60884 | 55.30713 | 39.09613 | 58 | 462 | 78.58969 | 29.41595 | 20.78284 |
| 59 | 344 | 90 | 21 | 19 | 59 | 869 | 100.2121 | 38.73676 | 33.71826 | 59 | 460 | 33.43822 | 28.32477 | 19.97998 |
| 60 | 344 | 180 | 21 | 19 | 60 | 840 | 102.7738 | 36.12372 | 31.91074 | 60 | 456 | 129.8357 | 26.375 | 22.79016 |
| 61 | 344 | 180 | 21 | 19 | 61 | 832 | 15.26862 | 46.65771 | 24.90759 | 61 | 454 | 16.58392 | 25.67261 | 21.73682 |
| 62 | 344 | 180 | 21 | 19 | 62 | 796 | 99.71647 | 35.73334 | 28.66492 | 62 | 451 | 143.2109 | 31.39264 | 20.18785 |
| 63 | 344 | 180 | 21 | 19 | 63 | 790 | 9.26252 | 47.81459 | 26.96988 | 63 | 442 | 148.8864 | 34.80823 | 15.7805 |
| 64 | 344 | 90 | 21 | 19 | 64 | 789 | 2.68695 | 42.14136 | 31.43471 | 64 | 433 | 41.03456 | 25.12958 | 23.06224 |
| 65 | 344 | 180 | 21 | 19 | 65 | 769 | 168.3995 | 47.44757 | 26.47437 | 65 | 431 | 152.1994 | 41.12445 | 13.41328 |
| 66 | 344 | 180 | 21 | 19 | 66 | 768 | 72.61831 | 35.07794 | 31.7999 | 66 | 430 | 159.5077 | 31.25232 | 17.33408 |
| 67 | 344 | 90 | 21 | 19 | 67 | 764 | 17.26376 | 37.64264 | 24.53192 | 67 | 430 | 170.2187 | 36.32611 | 17.70447 |
| 68 | 344 | 180 | 21 | 19 | 68 | 745 | 6.9045 | 42.29651 | 32.6405 | 68 | 424 | 152.0996 | 30.88062 | 21.67929 |
| 69 | 344 | 180 | 21 | 19 | 69 | 739 | 86.89257 | 50.49133 | 25.36548 | 69 | 417 | 104.6625 | 30.08057 | 17.96509 |
| 70 | 344 | 90 | 21 | 19 | 70 | 731 | 42.79077 | 56.85358 | 28.20873 | 70 | 406 | 178.242 | 27.20206 | 16.39128 |
| 71 | 314 | 90 | 19 | 19 | 71 | 722 | 26.26138 | 34.42548 | 31.31636 | 71 | 406 | 111.8664 | 27.10895 | 18.93354 |
| 72 | 314 | 90 | 19 | 19 | 72 | 719 | 103.7515 | 36.55011 | 27.05398 | 72 | 396 | 120.7485 | 24.71625 | 21.27856 |
| 73 | 314 | 90 | 19 | 19 | 73 | 716 | 34.97627 | 40.30862 | 30.14548 | 73 | 392 | 92.41044 | 24.3573 | 22.1067 |
| 74 | 314 | 90 | 19 | 19 | 74 | 694 | 71.50314 | 37.00238 | 25.30162 | 74 | 388 | 107.5166 | 27.50323 | 18.01758 |
| 75 | 314 | 90 | 19 | 19 | 75 | 685 | 64.38512 | 33.10406 | 26.82913 | 75 | 377 | 139.8837 | 23.91199 | 18.51648 |
| 76 | 314 | 90 | 19 | 19 | 76 | 652 | 90.84727 | 39.08447 | 36.98117 | 76 | 377 | 69.59625 | 27.61508 | 21.31696 |
| 77 | 314 | 90 | 19 | 19 | 77 | 609 | 63.19698 | 41.59238 | 21.90958 | 77 | 376 | 12.93845 | 25.32678 | 21.73125 |
| 78 | 314 | 90 | 19 | 19 | 78 | 602 | 1.01415 | 37.0473 | 26.17291 | 78 | 374 | 48.752 | 24.74197 | 20.41583 |
| 79 | 314 | 90 | 19 | 19 | 79 | 597 | 96.27859 | 33.12042 | 24.07477 | 79 | 372 | 113.1076 | 24.552 | 19.84247 |
| 80 | 314 | 90 | 19 | 19 | 80 | 591 | 139.4407 | 31.56 | 25.37943 | 80 | 372 | 42.38636 | 23.66492 | 19.29776 |
| 81 | 314 | 90 | 19 | 19 | 81 | 589 | 80.51788 | 43.56567 | 19.73094 | 81 | 369 | 31.49225 | 25.1665 | 19.14377 |
| 82 | 314 | 90 | 19 | 19 | 82 | 579 | 44.59735 | 33.28784 | 21.33197 | 82 | 368 | 170.0638 | 28.78787 | 16.4502 |
| 83 | 314 | 90 | 19 | 19 | 83 | 557 | 125.6044 | 34.1684 | 21.28995 | 83 | 362 | 35.69345 | 26.97375 | 20.42979 |
| 84 | 314 | 90 | 19 | 19 | 84 | 533 | 107.3292 | 32.93036 | 30.12759 | 84 | 357 | 72.23466 | 24.03906 | 21.56116 |
| 85 | 314 | 90 | 19 | 19 | 85 | 529 | 58.21991 | 34.49258 | 22.30521 | 85 | 356 | 133.7856 | 22.74225 | 19.28241 |
| 86 | 314 | 90 | 19 | 19 | 86 | 523 | 24.19505 | 28.72668 | 24.07339 | 86 | 350 | 10.66128 | 24.08295 | 19.1693 |
| 87 | 314 | 90 | 19 | 19 | 87 | 521 | 27.81589 | 29.52859 | 25.0087 | 87 | 349 | 31.79601 | 22.67529 | 19.51391 |
| 88 | 314 | 90 | 19 | 19 | 88 | 510 | 159.4036 | 33.82422 | 20.00949 | 88 | 346 | 165.7826 | 26.92285 | 17.22913 |
| 89 | 314 | 90 | 19 | 19 | 89 | 504 | 177.6395 | 34.88794 | 22.51675 | 89 | 346 | 144.0112 | 22.50195 | 18.31164 |
| 90 | 314 | 90 | 19 | 19 | 90 | 503 | 151.8556 | 29.4679 | 23.17233 | 90 | 344 | 70.26888 | 26.83673 | 16.48256 |
| 91 | 314 | 90 | 19 | 19 | 91 | 493 | 89.4077 | 28.06052 | 22.00922 | 91 | 342 | 1.34867 | 28.03931 | 14.23148 |
| 92 | 314 | 90 | 19 | 19 | 92 | 487 | 110.8897 | 26.43042 | 24.39044 | 92 | 342 | 88.20458 | 24.08221 | 17.33629 |
| 93 | 314 | 90 | 19 | 19 | 93 | 486 | 118.4762 | 32.01746 | 23.70406 | 93 | 336 | 151.973 | 28.23376 | 15.00635 |
| 94 | 314 | 90 | 19 | 19 | 94 | 479 | 129.3726 | 26.6609 | 23.07306 | 94 | 330 | 47.55389 | 22.16385 | 18.24049 |
| 95 | 314 | 90 | 19 | 19 | 95 | 452 | 67.49991 | 34.76318 | 18.89877 | 95 | 323 | 29.88286 | 26.05023 | 15.51627 |
| 96 | 314 | 90 | 19 | 19 | 96 | 442 | 89.68797 | 29.01587 | 23.01056 | 96 | 316 | 2.96804 | 22.22939 | 17.18427 |
| 97 | 314 | 90 | 19 | 19 | 97 | 437 | 17.80777 | 31.62088 | 27.47211 | 97 | 308 | 149.9662 | 24.32178 | 17.81512 |
| 98 | 314 | 90 | 19 | 19 | 98 | 411 | 79.70654 | 24.23804 | 22.36069 | 98 | 308 | 130.7258 | 22.79532 | 20.37633 |
| 99 | 312 | 90 | 19 | 19 | 99 | 400 | 23.15711 | 28.89008 | 24.03259 | 99 | 302 | 158.7375 | 21.953 | 21.5397 |
| 100 | 312 | 90 | 19 | 19 | 100 | 399 | 166.3697 | 29.80364 | 20.9675 | 100 | 300 | 174.1003 | 31.24695 | 17.11553 |
| 101 | 285 | 178.5051 | 19.12396 | 17.12465 | 101 | 387 | 107.1958 | 27.65741 | 18.01392 | 101 | 300 | 144.2268 | 22.88388 | 18.46937 |
| 102 | 285 | 178.5051 | 19.12396 | 17.12463 | 102 | 381 | 104.7084 | 28.40031 | 18.93353 | 102 | 288 | 28.42448 | 23.63181 | 15.09569 |
| 103 | 285 | 178.5051 | 19.12396 | 17.12469 | 103 | 380 | 88.36651 | 30.18732 | 18.22073 | 103 | 287 | 170.331 | 22.52725 | 16.29852 |
| 104 | 285 | 178.5051 | 19.12396 | 17.12469 | 104 | 379 | 62.33725 | 32.47778 | 17.45689 | 104 | 284 | 129.2939 | 25.32971 | 19.06757 |
| 105 | 285 | 178.5051 | 19.12396 | 17.12465 | 105 | 371 | 21.37976 | 25.26477 | 20.24434 | 105 | 280 | 41.89371 | 21.56519 | 14.14334 |
| 106 | 284 | 90 | 19 | 17 | 106 | 371 | 80.71279 | 35.6709 | 13.81649 | 106 | 276 | 138.5616 | 21.26007 | 17.11349 |
| 107 | 284 | 90 | 19 | 17 | 107 | 369 | 125.5402 | 25.22571 | 22.31971 | 107 | 275 | 111.3367 | 25.62964 | 17.97424 |
| 108 | 284 | 90 | 19 | 17 | 108 | 357 | 72.25814 | 27.16299 | 17.67688 | 108 | 273 | 51.20837 | 19.82104 | 15.45038 |
| 109 | 256 | 90 | 17 | 17 | 109 | 347 | 100.0531 | 30.23764 | 18.99467 | 109 | 272 | 29.33712 | 23.96985 | 14.38058 |
| 110 | 256 | 90 | 17 | 17 | 110 | 342 | 61.4824 | 26.01476 | 17.17218 | 110 | 271 | 150.5022 | 21.19739 | 15.63202 |
| 111 | 256 | 90 | 17 | 17 | 111 | 329 | 65.54389 | 25.49037 | 18.95129 | 111 | 269 | 85.19893 | 20.26462 | 18.60638 |
| 112 | 256 | 90 | 17 | 17 | 112 | 327 | 62.42252 | 21.89426 | 19.698 | 112 | 268 | 34.967 | 22.94019 | 15.40411 |
| 113 | 256 | 90 | 17 | 17 | 113 | 315 | 149.0001 | 26.7525 | 23.83517 | 113 | 260 | 62.4528 | 21.93323 | 17.96257 |
| 114 | 256 | 90 | 17 | 17 | 114 | 313 | 125.4371 | 29.53583 | 14.66556 | 114 | 259 | 121.8317 | 19.48364 | 17.90137 |
| 115 | 256 | 90 | 17 | 17 | 115 | 308 | 78.12807 | 22.81378 | 20.60083 | 115 | 259 | 41.51951 | 19.67664 | 16.4481 |
| 116 | 248 | 90 | 19 | 15 | 116 | 293 | 87.94746 | 24.94812 | 16.7742 | 116 | 256 | 114.1257 | 24.66962 | 13.5946 |
| 117 | 248 | 90 | 19 | 15 | 117 | 278 | 106.1202 | 21.56262 | 19.34135 | 117 | 252 | 163.6127 | 21.83966 | 17.21194 |
| 118 | 224 | 90 | 17 | 15 | 118 | 274 | 127.1258 | 26.78815 | 14.56772 | 118 | 250 | 138.8325 | 24.36597 | 12.23029 |
| 119 | 224 | 90 | 17 | 15 | 119 | 273 | 119.4336 | 21.84119 | 15.20956 | 119 | 247 | 25.94465 | 22.40778 | 13.94998 |
| 120 | 208 | 90 | 15 | 15 | 120 | 263 | 106.3239 | 24.76703 | 19.96857 | 120 | 246 | 158.5195 | 27.12358 | 12.12726 |
| 121 | 208 | 90 | 15 | 15 | 121 | 255 | 105.6152 | 25.8479 | 11.86823 | 121 | 245 | 120.0836 | 22.81976 | 14.53088 |
| 122 | 208 | 90 | 15 | 15 | 122 | 254 | 85.82309 | 19.60504 | 16.80917 | 122 | 243 | 174.6803 | 18.38602 | 16.30194 |
| 123 | 208 | 90 | 15 | 15 | 123 | 247 | 118.1331 | 24.52631 | 13.45456 | 123 | 240 | 120.9573 | 22.63751 | 13.89073 |
| 124 | 208 | 90 | 15 | 15 | 124 | 244 | 91.15097 | 20.07629 | 18.11688 | 124 | 239 | 79.31702 | 23.71362 | 12.84848 |
| 125 | 208 | 90 | 15 | 15 | 125 | 234 | 62.4339 | 18.04207 | 15.34357 | 125 | 221 | 173.3637 | 18.8727 | 15.01508 |
| 126 | 176 | 90 | 15 | 13 | 126 | 232 | 13.49873 | 19.37018 | 15.01379 | 126 | 219 | 172.9556 | 21.08679 | 14.13959 |
|  |  |  |  |  | 127 | 222 | 172.5046 | 21.86414 | 14.32382 | 127 | 211 | 16.29719 | 19.80231 | 14.2793 |
|  |  |  |  |  | 128 | 194 | 132.3893 | 20.83911 | 10.75664 | 128 | 211 | 21.87079 | 20.24011 | 13.55441 |
|  |  |  |  |  | 129 | 192 | 44.81573 | 22.61816 | 12.03213 | 129 | 205 | 119.0316 | 18.74632 | 14.27832 |
|  |  |  |  |  | 130 | 187 | 109.0332 | 20.24408 | 12.38837 | 130 | 199 | 25.22953 | 19.26666 | 13.7869 |
|  |  |  |  |  | 131 | 180 | 4.78158 | 25.07971 | 8.3056 | 131 | 196 | 151.0249 | 16.90387 | 15.74693 |
|  |  |  |  |  | 132 | 164 | 136.3014 | 19.1673 | 10.74841 | 132 | 193 | 71.21966 | 19.29529 | 15.16724 |
|  |  |  |  |  | 133 | 160 | 127.3661 | 16.58899 | 12.19604 | 133 | 190 | 93.96064 | 16.23807 | 14.31192 |
|  |  |  |  |  | 134 | 154 | 162.7793 | 18.6734 | 9.84776 | 134 | 180 | 14.12861 | 18.18781 | 13.09494 |
|  |  |  |  |  | 135 | 144 | 60.3303 | 18.11511 | 12.28561 | 135 | 144 | 175.046 | 17.19556 | 9.87628 |
|  |  |  |  |  | 136 | 140 | 127.4481 | 15.6073 | 12.3812 | 136 | 138 | 133.5011 | 14.1003 | 13.44894 |
|  |  |  |  |  | 137 | 140 | 100.7275 | 13.51736 | 12.53479 | 137 | 132 | 121.9648 | 15.05365 | 11.13071 |
|  |  |  |  |  | 138 | 133 | 59.53166 | 18.70895 | 9.68463 | 138 | 119 | 168.0226 | 13.96213 | 10.6124 |
|  |  |  |  |  | 139 | 130 | 116.0961 | 13.87415 | 12.53619 |  |  |  |  |  |
|  |  |  |  |  | 140 | 109 | 72.68745 | 14.55608 | 8.76596 |  |  |  |  |  |

Table S3. Particle size distribution of there kinds of NPs with different particle sizes.

| 80 nm Commercialized NPs |  | 50-100 nm Self-made NPs |  | 100-200 nm Self-made NPs |  | 200-400 nm Self-made NPs |  | 50-100 nm Naturally-derived NPs |  | 100-200 nm Naturally-derived NPs |  | 200-400 nm Naturally-derived NPs |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Size | Intensity | Size | Intensity | Size | Intensity | Size | Intensity | Size | Intensity | Size | Intensity | Size | Intensity |
| d.nm | counts | d.nm | counts | d.nm | counts | d.nm | counts | d.nm | counts | d.nm | counts | d.nm | counts |
| 0.4 | 0 | 0.4 | 0 | 0.4 | 0 | 0.4 | 0 | 0.4 | 0 | 0.4 | 0 | 0.4 | 0 |
| 0.463 | 0 | 0.463 | 0 | 0.463 | 0 | 0.463 | 0 | 0.463 | 0 | 0.463 | 0 | 0.463 | 0 |
| 0.536 | 0 | 0.536 | 0 | 0.536 | 0 | 0.536 | 0 | 0.536 | 0 | 0.536 | 0 | 0.536 | 0 |
| 0.621 | 0 | 0.621 | 0 | 0.621 | 0 | 0.621 | 0 | 0.621 | 0 | 0.621 | 0 | 0.621 | 0 |
| 0.719 | 0 | 0.719 | 0 | 0.719 | 0 | 0.719 | 0 | 0.719 | 0 | 0.719 | 0 | 0.719 | 0 |
| 0.833 | 0 | 0.833 | 0 | 0.833 | 0 | 0.833 | 0 | 0.833 | 0 | 0.833 | 0 | 0.833 | 0 |
| 0.965 | 0 | 0.965 | 0 | 0.965 | 0 | 0.965 | 0 | 0.965 | 0 | 0.965 | 0 | 0.965 | 0 |
| 1.12 | 0 | 1.12 | 0 | 1.12 | 0 | 1.12 | 0 | 1.12 | 0 | 1.12 | 0 | 1.12 | 0 |
| 1.29 | 0 | 1.29 | 0 | 1.29 | 0 | 1.29 | 0 | 1.29 | 0 | 1.29 | 0 | 1.29 | 0 |
| 1.5 | 0 | 1.5 | 0 | 1.5 | 0 | 1.5 | 0 | 1.5 | 0 | 1.5 | 0 | 1.5 | 0 |
| 1.74 | 0 | 1.74 | 0 | 1.74 | 0 | 1.74 | 0 | 1.74 | 0 | 1.74 | 0 | 1.74 | 0 |
| 2.01 | 0 | 2.01 | 0 | 2.01 | 0 | 2.01 | 0 | 2.01 | 0 | 2.01 | 0 | 2.01 | 0 |
| 2.33 | 0 | 2.33 | 0 | 2.33 | 0 | 2.33 | 0 | 2.33 | 0 | 2.33 | 0 | 2.33 | 0 |
| 2.7 | 0 | 2.7 | 0 | 2.7 | 0 | 2.7 | 0 | 2.7 | 0 | 2.7 | 0 | 2.7 | 0 |
| 3.12 | 0 | 3.12 | 0 | 3.12 | 0 | 3.12 | 0 | 3.12 | 0 | 3.12 | 0 | 3.12 | 0 |
| 3.62 | 0 | 3.62 | 0 | 3.62 | 0 | 3.62 | 0 | 3.62 | 0 | 3.62 | 0 | 3.62 | 0 |
| 4.19 | 0 | 4.19 | 0 | 4.19 | 0 | 4.19 | 0 | 4.19 | 0 | 4.19 | 0 | 4.19 | 0 |
| 4.85 | 0 | 4.85 | 0 | 4.85 | 0 | 4.85 | 0 | 4.85 | 0 | 4.85 | 0 | 4.85 | 0 |
| 5.61 | 0 | 5.61 | 0 | 5.61 | 0 | 5.61 | 0 | 5.61 | 0 | 5.61 | 0 | 5.61 | 0 |
| 6.5 | 0 | 6.5 | 0 | 6.5 | 0 | 6.5 | 0 | 6.5 | 0 | 6.5 | 0 | 6.5 | 0 |
| 7.53 | 0 | 7.53 | 0 | 7.53 | 0 | 7.53 | 0 | 7.53 | 0 | 7.53 | 0 | 7.53 | 0 |
| 8.72 | 0 | 8.72 | 0 | 8.72 | 0 | 8.72 | 0 | 8.72 | 0 | 8.72 | 0 | 8.72 | 0 |
| 10.1 | 0 | 10.1 | 0 | 10.1 | 0 | 10.1 | 0 | 10.1 | 0 | 10.1 | 0 | 10.1 | 0 |
| 11.7 | 0 | 11.7 | 0 | 11.7 | 0 | 11.7 | 0 | 11.7 | 0 | 11.7 | 0 | 11.7 | 0 |
| 13.5 | 0 | 13.5 | 0 | 13.5 | 0 | 13.5 | 0 | 13.5 | 0 | 13.5 | 0 | 13.5 | 0 |
| 15.7 | 0 | 15.7 | 0 | 15.7 | 0 | 15.7 | 0 | 15.7 | 0 | 15.7 | 0 | 15.7 | 0 |
| 18.2 | 0 | 18.2 | 0 | 18.2 | 0 | 18.2 | 0 | 18.2 | 0 | 18.2 | 0 | 18.2 | 0 |
| 21 | 0 | 21 | 0 | 21 | 0 | 21 | 0 | 21 | 0 | 21 | 0 | 21 | 0 |
| 24.4 | 0 | 24.4 | 0 | 24.4 | 0 | 24.4 | 0 | 24.4 | 0 | 24.4 | 0 | 24.4 | 0 |
| 28.2 | 0 | 28.2 | 0 | 28.2 | 0 | 28.2 | 0 | 28.2 | 0 | 28.2 | 0 | 28.2 | 0 |
| 32.7 | 0 | 32.7 | 0 | 32.7 | 0 | 32.7 | 0 | 32.7 | 0.0483 | 32.7 | 0 | 32.7 | 0 |
| 37.8 | 0 | 37.8 | 0 | 37.8 | 0 | 37.8 | 0 | 37.8 | 0.106 | 37.8 | 0 | 37.8 | 0 |
| 43.8 | 0 | 43.8 | 0 | 43.8 | 0.0895 | 43.8 | 0 | 43.8 | 0.122 | 43.8 | 0 | 43.8 | 0 |
| 50.7 | 1.21 | 50.7 | 0 | 50.7 | 0.986 | 50.7 | 0 | 50.7 | 0.188 | 50.7 | 0 | 50.7 | 0 |
| 58.8 | 6.48 | 58.8 | 0 | 58.8 | 3.15 | 58.8 | 0.0245 | 58.8 | 0.478 | 58.8 | 0.0139 | 58.8 | 0.0592 |
| 68.1 | 13.7 | 68.1 | 0 | 68.1 | 6.06 | 68.1 | 0.126 | 68.1 | 0.725 | 68.1 | 0.622 | 68.1 | 0.462 |
| 78.8 | 19.4 | 78.8 | 0 | 78.8 | 8.94 | 78.8 | 0.312 | 78.8 | 1.32 | 78.8 | 2.08 | 78.8 | 1.34 |
| 91.3 | 21.2 | 91.3 | 0 | 91.3 | 11.1 | 91.3 | 0.803 | 91.3 | 1.86 | 91.3 | 3.38 | 91.3 | 2.99 |
| 106 | 18.4 | 106 | 0.151 | 106 | 12.2 | 106 | 2.08 | 106 | 1.93 | 106 | 3.55 | 106 | 5.28 |
| 122 | 12.4 | 122 | 1.76 | 122 | 12.2 | 122 | 4.09 | 122 | 1.59 | 122 | 2.48 | 122 | 7.79 |
| 142 | 5.82 | 142 | 3.6 | 142 | 11.1 | 142 | 6.46 | 142 | 1.32 | 142 | 0.937 | 142 | 10 |
| 164 | 1.27 | 164 | 4.31 | 164 | 9.34 | 164 | 8.77 | 164 | 1.62 | 164 | 0 | 164 | 11.5 |
| 190 | 0 | 190 | 3.74 | 190 | 7.19 | 190 | 10.6 | 190 | 2.25 | 190 | 7.11 | 190 | 11.9 |
| 220 | 0 | 220 | 2.8 | 220 | 5.02 | 220 | 11.7 | 220 | 2.55 | 220 | 14.8 | 220 | 11.3 |
| 255 | 0 | 255 | 2.09 | 255 | 3.09 | 255 | 11.8 | 255 | 2.4 | 255 | 12.7 | 255 | 9.76 |
| 295 | 0 | 295 | 1.35 | 295 | 1.6 | 295 | 11 | 295 | 1.91 | 295 | 6.04 | 295 | 7.68 |
| 342 | 0 | 342 | 0.899 | 342 | 0.633 | 342 | 9.46 | 342 | 1.41 | 342 | 10.4 | 342 | 5.5 |
| 396 | 0 | 396 | 0.786 | 396 | 0.15 | 396 | 7.36 | 396 | 1.2 | 396 | 13.3 | 396 | 3.65 |
| 459 | 0 | 459 | 1.1 | 459 | 0.0249 | 459 | 5.06 | 459 | 3.46 | 459 | 12.3 | 459 | 2.34 |
| 531 | 0 | 531 | 2.16 | 531 | 0.0422 | 531 | 2.93 | 531 | 7.82 | 531 | 7.73 | 531 | 1.47 |
| 615 | 0 | 615 | 4.2 | 615 | 0.102 | 615 | 1.29 | 615 | 12 | 615 | 2.39 | 615 | 0.821 |
| 712 | 0 | 712 | 8.47 | 712 | 0.159 | 712 | 0.332 | 712 | 13.2 | 712 | 0 | 712 | 0.403 |
| 825 | 0 | 825 | 13 | 825 | 0.184 | 825 | 0.0317 | 825 | 10.6 | 825 | 0 | 825 | 0.158 |
| 955 | 0 | 955 | 15.3 | 955 | 0.168 | 955 | 0.0469 | 955 | 5.73 | 955 | 0 | 955 | 0.0254 |
| 1110 | 0 | 1110 | 13.7 | 1110 | 0.12 | 1110 | 0.108 | 1110 | 2.09 | 1110 | 0 | 1110 | 0 |
| 1280 | 0 | 1280 | 9.25 | 1280 | 0.0601 | 1280 | 0.155 | 1280 | 2.07 | 1280 | 0 | 1280 | 0 |
| 1480 | 0 | 1480 | 4.39 | 1480 | 0.0141 | 1480 | 0.173 | 1480 | 3.19 | 1480 | 0 | 1480 | 0 |
| 1720 | 0 | 1720 | 1.75 | 1720 | 3.04E-04 | 1720 | 0.164 | 1720 | 3.88 | 1720 | 0 | 1720 | 0 |
| 1990 | 0 | 1990 | 0.764 | 1990 | 0.0198 | 1990 | 0.142 | 1990 | 3.86 | 1990 | 0 | 1990 | 0 |
| 2300 | 0 | 2300 | 0.239 | 2300 | 0.0668 | 2300 | 0.129 | 2300 | 3.12 | 2300 | 0 | 2300 | 0 |
| 2670 | 0 | 2670 | 0 | 2670 | 0.161 | 2670 | 0.148 | 2670 | 1.94 | 2670 | 0 | 2670 | 0 |
| 3090 | 0 | 3090 | 0 | 3090 | 0.384 | 3090 | 0.219 | 3090 | 0.741 | 3090 | 0 | 3090 | 0 |
| 3580 | 0 | 3580 | 0 | 3580 | 0.747 | 3580 | 0.343 | 3580 | 0 | 3580 | 0 | 3580 | 0.0705 |
| 4150 | 0 | 4150 | 0.088 | 4150 | 1.2 | 4150 | 0.654 | 4150 | 0 | 4150 | 0 | 4150 | 0.371 |
| 4800 | 0 | 4800 | 0.787 | 4800 | 1.65 | 4800 | 1.32 | 4800 | 0.877 | 4800 | 0 | 4800 | 1.57 |
| 5560 | 0 | 5560 | 3.29 | 5560 | 1.98 | 5560 | 2.17 | 5560 | 2.47 | 5560 | 0 | 5560 | 3.51 |
| 6440 | 0 | 6440 | 0 | 6440 | 0 | 6440 | 0 | 6440 | 0 | 6440 | 0 | 6440 | 0 |
| 7460 | 0 | 7460 | 0 | 7460 | 0 | 7460 | 0 | 7460 | 0 | 7460 | 0 | 7460 | 0 |
| 8630 | 0 | 8630 | 0 | 8630 | 0 | 8630 | 0 | 8630 | 0 | 8630 | 0 | 8630 | 0 |

Table S4. Zeta potential of there kinds of NPs with different particle sizes.

| Groups | Zeta potential |  |  |
| --- | --- | --- | --- |
| Control | -3.42 | -1.79 | -3.52 |
| 80 nm PS NPs | -43.5 | -45.8 | -45.6 |
| 50~100 nm Self-made NPs | -30.5 | -25.9 | -24.8 |
| 100~200 nm Self-made NPs | -30.5 | -31.1 | -30.5 |
| 200~400 nm Self-made NPs | -24 | -28.7 | -27.7 |
| 50-100 nm Naturally-derived NPs | -33.7 | -33.3 | -41.7 |
| 100-200 nm Naturally-derived NPs | -20.4 | -21.3 | -22.6 |
| 200-400 nm Naturally-derived NPs | -47.3 | -43.8 | -41 |

Table S5. Raman spectrum information of the three kinds of NPs.

| Raman shift | Intensity | Raman shift | Intensity | Raman shift | Intensity | Raman shift | Intensity | Raman shift | Intensity | Raman shift | Intensity | Raman shift | Intensity |  | Raman shift | Intensity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| control |  | PS NPs |  | 50-100 nm PP NPs |  | 100-200 nm PP NPs |  | 200-400 nm PP NPs |  | 50-100 nmNaturally-derived NPs |  | 100-200 nmNaturally-derived NPs |  | 200-400 nmNaturally-derived NPs |  |  |
| 600.181 | 0 | 600.502 | 36.00755 | 600.284 | 0 | 600.284 | 0 | 600.284 | 0 | 600.284 | 0 | 600.284 | 0 |  | 600.284 | 0 |
| 600.916 | 1.36254 | 601.238 | 36.74855 | 601.022 | 61.7345 | 601.022 | 3.02767 | 601.022 | 27.7032 | 601.022 | 2.67972 | 601.022 | 27.23013 |  | 601.022 | 62.01522 |
| 601.652 | 2.71405 | 601.975 | 35.02755 | 601.76 | 62.73638 | 601.76 | 23.09208 | 601.76 | 50.81838 | 601.76 | 22.39618 | 601.76 | 49.87223 |  | 601.76 | 63.29783 |
| 602.389 | 4.00495 | 602.713 | 35.18018 | 602.496 | 73.36806 | 602.496 | 41.00991 | 602.496 | 52.21485 | 602.496 | 39.967 | 602.496 | 50.79692 |  | 602.496 | 74.20947 |
| 603.125 | 5.25879 | 603.449 | 34.963 | 603.233 | 76.92268 | 603.233 | 53.27456 | 603.233 | 56.38089 | 603.233 | 51.88418 | 603.233 | 54.49053 |  | 603.233 | 78.04442 |
| 603.861 | 6.49062 | 604.186 | 35.56482 | 603.971 | 85.56363 | 603.971 | 56.8922 | 603.971 | 68.89685 | 603.971 | 55.15387 | 603.971 | 66.53342 |  | 603.971 | 86.96609 |
| 604.597 | 7.69585 | 604.924 | 35.305 | 604.708 | 91.14075 | 604.708 | 61.5163 | 604.708 | 76.29546 | 604.708 | 59.43049 | 604.708 | 73.45959 |  | 604.708 | 92.82356 |
| 605.333 | 8.8428 | 605.66 | 35.00964 | 605.445 | 92.08564 | 605.445 | 69.31533 | 605.445 | 81.51836 | 605.445 | 66.88204 | 605.445 | 78.21006 |  | 605.445 | 94.04879 |
| 606.068 | 9.93406 | 606.397 | 34.77036 | 606.182 | 96.64043 | 606.182 | 74.65956 | 606.182 | 84.88243 | 606.182 | 71.87879 | 606.182 | 81.1017 |  | 606.182 | 98.88392 |
| 606.804 | 10.95935 | 607.134 | 32.77655 | 606.92 | 102.7032 | 606.92 | 77.58677 | 606.92 | 87.75162 | 606.92 | 74.45805 | 606.92 | 83.49781 |  | 606.92 | 105.2274 |
| 607.54 | 11.90381 | 607.869 | 32.61118 | 607.657 | 104.1954 | 607.657 | 83.22178 | 607.657 | 92.0426 | 607.657 | 79.74559 | 607.657 | 87.31637 |  | 607.657 | 106.9999 |
| 608.275 | 12.77463 | 608.606 | 33.30673 | 608.392 | 108.853 | 608.392 | 87.0017 | 608.392 | 97.64133 | 608.392 | 83.17897 | 608.392 | 92.44394 |  | 608.392 | 111.9372 |
| 609.011 | 13.57484 | 609.342 | 34.29227 | 609.129 | 111.8133 | 609.129 | 91.22565 | 609.129 | 103.594 | 609.129 | 87.05545 | 609.129 | 97.92413 |  | 609.129 | 115.1778 |
| 609.746 | 14.30355 | 610.079 | 36.09855 | 609.866 | 113.7567 | 609.866 | 92.00876 | 609.866 | 109.5968 | 609.866 | 87.49107 | 609.866 | 103.4546 |  | 609.866 | 117.4015 |
| 610.482 | 14.97256 | 610.815 | 36.60891 | 610.603 | 115.1617 | 610.603 | 94.37663 | 610.603 | 114.126 | 610.603 | 89.51147 | 610.603 | 107.5113 |  | 610.603 | 119.0868 |
| 611.215 | 15.59103 | 611.551 | 37.31982 | 611.339 | 118.0356 | 611.339 | 99.60324 | 611.339 | 119.9372 | 611.339 | 94.39107 | 611.339 | 112.8507 |  | 611.339 | 122.2408 |
| 611.951 | 16.1677 | 612.287 | 39.98618 | 612.076 | 118.5561 | 612.076 | 103.8013 | 612.076 | 123.222 | 612.076 | 98.24166 | 612.076 | 115.6631 |  | 612.076 | 123.0416 |
| 612.686 | 16.70471 | 613.024 | 41.22055 | 612.813 | 120.8059 | 612.813 | 108.1927 | 612.813 | 126.9709 | 612.813 | 102.2856 | 612.813 | 118.9396 |  | 612.813 | 125.5717 |
| 613.421 | 17.19857 | 613.759 | 40.81745 | 613.548 | 122.8866 | 613.548 | 109.341 | 613.548 | 129.1156 | 613.548 | 103.0873 | 613.548 | 120.6131 |  | 613.548 | 127.932 |
| 614.156 | 17.65235 | 614.495 | 41.61018 | 614.284 | 125.564 | 614.284 | 111.6626 | 614.284 | 131.0636 | 614.284 | 105.0619 | 614.284 | 122.0893 |  | 614.284 | 130.8894 |
| 614.891 | 18.06539 | 615.23 | 41.26882 | 615.02 | 129.49 | 615.02 | 115.0905 | 615.02 | 135.833 | 615.02 | 108.1429 | 615.02 | 126.3869 |  | 615.02 | 135.0953 |
| 615.626 | 18.44914 | 615.966 | 41.72009 | 615.757 | 133.1925 | 615.757 | 117.792 | 615.757 | 139.0796 | 615.757 | 110.4968 | 615.757 | 129.1611 |  | 615.757 | 139.0782 |
| 616.361 | 18.81112 | 616.703 | 41.92236 | 616.493 | 136.2601 | 616.493 | 122.4338 | 616.493 | 144.3402 | 616.493 | 114.7916 | 616.493 | 133.9499 |  | 616.493 | 142.4257 |
| 617.095 | 19.16301 | 617.437 | 41.52591 | 617.229 | 140.3259 | 617.229 | 127.1233 | 617.229 | 146.9062 | 617.229 | 119.1341 | 617.229 | 136.0442 |  | 617.229 | 146.7715 |
| 617.83 | 19.52094 | 618.173 | 40.75673 | 617.964 | 144.2318 | 617.964 | 130.7988 | 617.964 | 151.6394 | 617.964 | 122.4631 | 617.964 | 140.3062 |  | 617.964 | 150.9569 |
| 618.563 | 19.8962 | 618.908 | 39.62991 | 618.7 | 147.6753 | 618.7 | 135.3208 | 618.7 | 156.6966 | 618.7 | 126.6381 | 618.7 | 144.8916 |  | 618.7 | 154.6804 |
| 619.298 | 20.28745 | 619.644 | 40.35227 | 619.435 | 152.665 | 619.435 | 139.8945 | 619.435 | 162.2962 | 619.435 | 130.8652 | 619.435 | 150.0201 |  | 619.435 | 159.9497 |
| 620.032 | 20.69442 | 620.38 | 39.92018 | 620.171 | 155.9595 | 620.171 | 145.8641 | 620.171 | 167.5925 | 620.171 | 136.4878 | 620.171 | 154.8446 |  | 620.171 | 163.5242 |
| 620.766 | 21.11364 | 621.114 | 38.74927 | 620.907 | 158.7992 | 620.907 | 150.6601 | 620.907 | 172.3789 | 620.907 | 140.9368 | 620.907 | 159.1592 |  | 620.907 | 166.6438 |
| 621.501 | 21.53592 | 621.85 | 38.66073 | 621.641 | 162.4847 | 621.641 | 154.4896 | 621.641 | 175.9984 | 621.641 | 144.4203 | 621.641 | 162.3081 |  | 621.641 | 170.6085 |
| 622.235 | 21.95657 | 622.584 | 38.18227 | 622.377 | 166.7111 | 622.377 | 159.3232 | 622.377 | 179.2851 | 622.377 | 148.9068 | 622.377 | 165.1231 |  | 622.377 | 175.1148 |
| 622.969 | 22.37161 | 623.319 | 38.00745 | 623.113 | 169.5303 | 623.113 | 162.2124 | 623.113 | 184.5292 | 623.113 | 151.4491 | 623.113 | 169.8954 |  | 623.113 | 178.214 |
| 623.702 | 22.78231 | 624.053 | 37.44082 | 623.848 | 171.9236 | 623.848 | 165.5256 | 623.848 | 189.9965 | 623.848 | 154.4158 | 623.848 | 174.8916 |  | 623.848 | 180.8869 |
| 624.436 | 23.19102 | 624.789 | 35.99836 | 624.583 | 174.2077 | 624.583 | 168.3418 | 624.583 | 194.6022 | 624.583 | 156.8854 | 624.583 | 179.0261 |  | 624.583 | 183.4506 |
| 625.17 | 23.60113 | 625.523 | 35.75782 | 625.317 | 176.2782 | 625.317 | 170.5164 | 625.317 | 199.0298 | 625.317 | 158.714 | 625.317 | 182.9832 |  | 625.317 | 185.8003 |
| 625.904 | 24.01108 | 626.258 | 35.45464 | 626.053 | 177.9003 | 626.053 | 173.4961 | 626.053 | 202.0008 | 626.053 | 161.3467 | 626.053 | 185.4824 |  | 626.053 | 187.7023 |
| 626.637 | 24.41605 | 626.993 | 35.15618 | 626.788 | 179.4524 | 626.788 | 177.0329 | 626.788 | 204.7064 | 626.788 | 164.5369 | 626.788 | 187.7168 |  | 626.788 | 189.534 |
| 627.371 | 24.81237 | 627.727 | 33.23482 | 627.523 | 180.3983 | 627.523 | 178.7491 | 627.523 | 207.9644 | 627.523 | 165.9066 | 627.523 | 190.5037 |  | 627.523 | 190.7595 |
| 628.103 | 25.1987 | 628.462 | 33.23573 | 628.258 | 182.0732 | 628.258 | 181.1884 | 628.258 | 210.6027 | 628.258 | 167.9993 | 628.258 | 192.6708 |  | 628.258 | 192.714 |
| 628.837 | 25.57176 | 629.195 | 35.199 | 628.992 | 184.3097 | 628.992 | 182.7802 | 628.992 | 213.4345 | 628.992 | 169.2451 | 628.992 | 195.0321 |  | 628.992 | 195.2297 |
| 629.571 | 25.93087 | 629.93 | 36.04973 | 629.727 | 185.5956 | 629.727 | 183.8234 | 629.727 | 215.8773 | 629.727 | 169.9417 | 629.727 | 197.0038 |  | 629.727 | 196.7951 |
| 630.304 | 26.27423 | 630.664 | 36.54473 | 630.461 | 186.0702 | 630.461 | 185.8489 | 630.461 | 217.9904 | 630.461 | 171.6212 | 630.461 | 198.6464 |  | 630.461 | 197.5489 |
| 631.037 | 26.5969 | 631.398 | 37.85109 | 631.196 | 187.191 | 631.196 | 187.544 | 631.196 | 220.4485 | 631.196 | 172.9697 | 631.196 | 200.6333 |  | 631.196 | 198.9493 |
| 631.769 | 26.89226 | 632.132 | 38.56045 | 631.929 | 188.1628 | 631.929 | 188.7633 | 631.929 | 223.7821 | 631.929 | 173.8435 | 631.929 | 203.4971 |  | 631.929 | 200.2 |
| 632.503 | 27.15765 | 632.866 | 38.24882 | 632.664 | 188.9373 | 632.664 | 190.0426 | 632.664 | 227.4696 | 632.664 | 174.7762 | 632.664 | 206.7134 |  | 632.664 | 201.2541 |
| 633.236 | 27.39423 | 633.599 | 38.87764 | 633.399 | 190.2076 | 633.399 | 191.1474 | 633.399 | 230.2435 | 633.399 | 175.5345 | 633.399 | 209.0161 |  | 633.399 | 202.804 |
| 633.969 | 27.60334 | 634.334 | 39.37464 | 634.133 | 190.8412 | 634.133 | 191.6208 | 634.133 | 231.8662 | 634.133 | 175.6618 | 634.133 | 210.1684 |  | 634.133 | 203.7167 |
| 634.702 | 27.78763 | 635.067 | 40.17418 | 634.866 | 190.4519 | 634.866 | 192.6925 | 634.866 | 234.2918 | 634.866 | 176.3879 | 634.866 | 212.1241 |  | 634.866 | 203.6062 |
| 635.433 | 27.95007 | 635.801 | 41.87818 | 635.6 | 190.6176 | 635.6 | 193.784 | 635.6 | 235.541 | 635.6 | 177.1334 | 635.6 | 212.9028 |  | 635.6 | 204.0511 |
| 636.166 | 28.08977 | 636.534 | 41.70409 | 636.335 | 189.5581 | 636.335 | 193.1504 | 636.335 | 236.8622 | 636.335 | 176.1532 | 636.335 | 213.7528 |  | 636.335 | 203.2713 |
| 636.899 | 28.20714 | 637.268 | 40.23382 | 637.069 | 188.9405 | 637.069 | 193.9944 | 637.069 | 237.6485 | 637.069 | 176.6511 | 637.069 | 214.0686 |  | 637.069 | 202.9329 |
| 637.632 | 28.30322 | 638.001 | 39.89655 | 637.802 | 187.944 | 637.802 | 194.7222 | 637.802 | 239.2089 | 637.802 | 177.0333 | 637.802 | 215.1592 |  | 637.802 | 202.2151 |
| 638.364 | 28.37504 | 638.735 | 39.82591 | 638.536 | 188.5397 | 638.536 | 195.7094 | 638.536 | 239.503 | 638.536 | 177.6745 | 638.536 | 214.9828 |  | 638.536 | 203.0901 |
| 639.096 | 28.42299 | 639.468 | 40.43009 | 639.27 | 188.6742 | 639.27 | 196.5159 | 639.27 | 239.2226 | 639.27 | 178.1349 | 639.27 | 214.2318 |  | 639.27 | 203.5037 |
| 639.828 | 28.44999 | 640.201 | 41.002 | 640.004 | 188.3754 | 640.004 | 196.697 | 640.004 | 239.2708 | 640.004 | 177.97 | 640.004 | 213.8096 |  | 640.004 | 203.4842 |
| 640.561 | 28.45654 | 640.934 | 41.00255 | 640.736 | 188.0781 | 640.736 | 195.7755 | 640.736 | 239.0518 | 640.736 | 176.7034 | 640.736 | 213.1213 |  | 640.736 | 203.4653 |
| 641.293 | 28.44131 | 641.668 | 40.56809 | 641.47 | 186.9552 | 641.47 | 196.0652 | 641.47 | 238.5316 | 641.47 | 176.6469 | 641.47 | 212.1306 |  | 641.47 | 202.6216 |
| 642.024 | 28.3995 | 642.4 | 41.23091 | 642.203 | 187.3436 | 642.203 | 195.7855 | 642.203 | 239.1734 | 642.203 | 176.0217 | 642.203 | 212.3026 |  | 642.203 | 203.2888 |
| 642.756 | 28.33111 | 643.133 | 41.77355 | 642.936 | 186.4451 | 642.936 | 196.0746 | 642.936 | 239.0569 | 642.936 | 175.9652 | 642.936 | 211.7162 |  | 642.936 | 202.6691 |
| 643.488 | 28.23841 | 643.866 | 42.19336 | 643.669 | 185.9096 | 643.669 | 195.4025 | 643.669 | 239.4298 | 643.669 | 174.9475 | 643.669 | 211.6191 |  | 643.669 | 202.4125 |
| 644.22 | 28.12257 | 644.599 | 41.32809 | 644.403 | 184.8476 | 644.403 | 194.641 | 644.403 | 238.6666 | 644.403 | 173.84 | 644.403 | 210.3855 |  | 644.403 | 201.6296 |
| 644.951 | 27.9874 | 645.331 | 41.91218 | 645.136 | 183.6858 | 645.136 | 194.4829 | 645.136 | 239.7126 | 645.136 | 173.3363 | 645.136 | 210.9616 |  | 645.136 | 200.7467 |
| 645.683 | 27.83269 | 646.064 | 41.07027 | 645.868 | 183.4104 | 645.868 | 195.4573 | 645.868 | 240.6127 | 645.868 | 173.9655 | 645.868 | 211.3925 |  | 645.868 | 200.7497 |
| 646.415 | 27.65483 | 646.796 | 41.25255 | 646.601 | 182.0092 | 646.601 | 194.0964 | 646.601 | 241.9204 | 646.601 | 172.259 | 646.601 | 212.2303 |  | 646.601 | 199.6274 |
| 647.147 | 27.45547 | 647.529 | 40.10273 | 647.335 | 180.1551 | 647.335 | 193.5185 | 647.335 | 242.7307 | 647.335 | 171.3351 | 647.335 | 212.5701 |  | 647.335 | 198.0524 |
| 647.877 | 27.2379 | 648.261 | 38.65355 | 648.066 | 178.4659 | 648.066 | 192.9386 | 648.066 | 242.5977 | 648.066 | 170.4105 | 648.066 | 211.9685 |  | 648.066 | 196.6413 |
| 648.609 | 27.00464 | 648.994 | 38.95136 | 648.799 | 175.7849 | 648.799 | 193.2495 | 648.799 | 242.7848 | 648.799 | 170.3759 | 648.799 | 211.6857 |  | 648.799 | 194.2391 |
| 649.34 | 26.75804 | 649.726 | 39.14473 | 649.532 | 173.221 | 649.532 | 192.5173 | 649.532 | 244.2321 | 649.532 | 169.298 | 649.532 | 212.6632 |  | 649.532 | 191.954 |
| 650.072 | 26.5006 | 650.457 | 38.85182 | 650.264 | 172.1131 | 650.264 | 191.7744 | 650.264 | 243.7301 | 650.264 | 168.21 | 650.264 | 211.6919 |  | 650.264 | 191.1246 |
| 650.802 | 26.23434 | 651.19 | 39.50336 | 650.997 | 170.4698 | 650.997 | 189.0944 | 650.997 | 243.0091 | 650.997 | 165.1844 | 650.997 | 210.5012 |  | 650.997 | 189.7601 |
| 651.533 | 25.96436 | 651.922 | 37.30518 | 651.73 | 168.5394 | 651.73 | 187.4974 | 651.73 | 241.5089 | 651.73 | 163.2418 | 651.73 | 208.5311 |  | 651.73 | 188.1085 |
| 652.265 | 25.69486 | 652.654 | 36.92836 | 652.461 | 165.8044 | 652.461 | 184.7568 | 652.461 | 240.6032 | 652.461 | 160.1566 | 652.461 | 207.1568 |  | 652.461 | 185.6515 |
| 652.995 | 25.42894 | 653.385 | 36.84818 | 653.194 | 163.4245 | 653.194 | 183.5455 | 653.194 | 242.3671 | 653.194 | 158.5997 | 653.194 | 208.4508 |  | 653.194 | 183.5505 |
| 653.726 | 25.17126 | 654.118 | 37.49455 | 653.926 | 161.0609 | 653.926 | 182.6602 | 653.926 | 241.2489 | 653.926 | 157.3693 | 653.926 | 206.8634 |  | 653.926 | 181.4653 |
| 654.457 | 24.92834 | 654.849 | 36.94045 | 654.657 | 158.4391 | 654.657 | 180.5624 | 654.657 | 240.0919 | 654.657 | 154.9269 | 654.657 | 205.2378 |  | 654.657 | 179.1216 |
| 655.188 | 24.70243 | 655.581 | 37.09964 | 655.39 | 156.0923 | 655.39 | 178.0017 | 655.39 | 239.4514 | 655.39 | 152.0205 | 655.39 | 204.1275 |  | 655.39 | 177.0537 |
| 655.918 | 24.49279 | 656.312 | 39.387 | 656.122 | 154.401 | 656.122 | 174.9798 | 656.122 | 237.4065 | 656.122 | 148.6535 | 656.122 | 201.6133 |  | 656.122 | 175.6407 |
| 656.648 | 24.29712 | 657.043 | 40.11664 | 656.853 | 151.5834 | 656.853 | 172.8908 | 656.853 | 235.8545 | 656.853 | 146.2199 | 656.853 | 199.5927 |  | 656.853 | 173.1012 |
| 657.379 | 24.11269 | 657.775 | 39.56345 | 657.585 | 148.899 | 657.585 | 170.4175 | 657.585 | 234.3917 | 657.585 | 143.4014 | 657.585 | 197.6607 |  | 657.585 | 170.6952 |
| 658.109 | 23.94175 | 658.506 | 39.53836 | 658.317 | 146.4773 | 658.317 | 166.6813 | 658.317 | 232.3865 | 658.317 | 139.3202 | 658.317 | 195.1862 |  | 658.317 | 168.552 |
| 658.839 | 23.78497 | 659.238 | 38.21591 | 659.048 | 143.5226 | 659.048 | 163.3622 | 659.048 | 230.9122 | 659.048 | 135.6564 | 659.048 | 193.2434 |  | 659.048 | 165.8754 |
| 659.57 | 23.6413 | 659.969 | 39.61555 | 659.78 | 139.4649 | 659.78 | 160.0809 | 659.78 | 230.856 | 659.78 | 132.0299 | 659.78 | 192.7179 |  | 659.78 | 162.0961 |
| 660.299 | 23.51018 | 660.699 | 39.67273 | 660.512 | 136.8687 | 660.512 | 157.9348 | 660.512 | 227.4591 | 660.512 | 129.5388 | 660.512 | 188.8518 |  | 660.512 | 159.7783 |
| 661.03 | 23.38964 | 661.431 | 38.11364 | 661.242 | 134.3176 | 661.242 | 155.9788 | 661.242 | 224.3709 | 661.242 | 127.2385 | 661.242 | 185.2957 |  | 661.242 | 157.5049 |
| 661.76 | 23.28118 | 662.162 | 38.598 | 661.974 | 132.879 | 661.974 | 154.7455 | 661.974 | 222.8256 | 661.974 | 125.6602 | 661.974 | 183.2811 |  | 661.974 | 156.3447 |
| 662.489 | 23.1853 | 662.893 | 38.70018 | 662.704 | 130.2254 | 662.704 | 152.6002 | 662.704 | 220.5326 | 662.704 | 123.1707 | 662.704 | 180.5202 |  | 662.704 | 153.9688 |
| 663.219 | 23.0983 | 663.623 | 38.46318 | 663.436 | 127.0182 | 663.436 | 150.2168 | 663.436 | 218.4031 | 663.436 | 120.4421 | 663.436 | 177.9215 |  | 663.436 | 151.0401 |
| 663.949 | 23.01861 | 664.354 | 38.09391 | 664.168 | 124.7088 | 664.168 | 147.2817 | 664.168 | 216.9757 | 664.168 | 117.1619 | 664.168 | 176.0248 |  | 664.168 | 149.0091 |
| 664.678 | 22.94438 | 665.085 | 37.58073 | 664.898 | 122.1206 | 664.898 | 145.4974 | 664.898 | 214.7697 | 664.898 | 115.0335 | 664.898 | 173.3509 |  | 664.898 | 146.6986 |
| 665.408 | 22.87226 | 665.815 | 37.00018 | 665.629 | 119.1467 | 665.629 | 143.4035 | 665.629 | 212.9294 | 665.629 | 112.5949 | 665.629 | 171.042 |  | 665.629 | 144.0027 |
| 666.138 | 22.79855 | 666.545 | 38.11136 | 666.359 | 116.063 | 666.359 | 140.7427 | 666.359 | 211.5495 | 666.359 | 109.5899 | 666.359 | 169.1941 |  | 666.359 | 141.1967 |
| 666.867 | 22.72231 | 667.276 | 38.63455 | 667.09 | 113.7789 | 667.09 | 139.0921 | 667.09 | 210.9422 | 667.09 | 107.5946 | 667.09 | 168.1183 |  | 667.09 | 139.1906 |
| 667.597 | 22.64086 | 668.006 | 38.26318 | 667.822 | 112.5287 | 667.822 | 135.8528 | 667.822 | 210.2089 | 667.822 | 104.0103 | 667.822 | 166.9158 |  | 667.822 | 138.2189 |
| 668.325 | 22.55259 | 668.737 | 39.24355 | 668.551 | 109.742 | 668.551 | 132.8792 | 668.551 | 209.5341 | 668.551 | 100.693 | 668.551 | 165.7737 |  | 668.551 | 135.7096 |
| 669.055 | 22.45569 | 669.467 | 41.45391 | 669.282 | 107.2274 | 669.282 | 131.2861 | 669.282 | 207.756 | 669.282 | 98.75522 | 669.282 | 163.5269 |  | 669.282 | 133.473 |
| 669.784 | 22.34923 | 670.197 | 39.145 | 670.012 | 103.5716 | 670.012 | 129.6421 | 670.012 | 205.2955 | 670.012 | 96.76707 | 670.012 | 160.5985 |  | 670.012 | 130.0948 |
| 670.512 | 22.23066 | 670.928 | 38.10327 | 670.743 | 100.0015 | 670.743 | 127.1076 | 670.743 | 202.7887 | 670.743 | 93.88791 | 670.743 | 157.6232 |  | 670.743 | 126.8028 |
| 671.242 | 22.09609 | 671.657 | 37.35964 | 671.474 | 96.99366 | 671.474 | 125.6229 | 671.474 | 201.653 | 671.474 | 92.05848 | 671.474 | 156.0189 |  | 671.474 | 124.073 |
| 671.971 | 21.94299 | 672.386 | 35.28982 | 672.203 | 94.46278 | 672.203 | 123.0216 | 672.203 | 200.0307 | 672.203 | 89.11352 | 672.203 | 153.9292 |  | 672.203 | 121.8194 |
| 672.699 | 21.77113 | 673.117 | 35.69909 | 672.934 | 91.5236 | 672.934 | 120.8071 | 672.934 | 198.4489 | 672.934 | 86.55442 | 672.934 | 151.8789 |  | 672.934 | 119.1583 |
| 673.429 | 21.58133 | 673.846 | 36.61382 | 673.663 | 90.15877 | 673.663 | 120.1746 | 673.663 | 195.3688 | 673.663 | 85.57814 | 673.663 | 148.3315 |  | 673.663 | 118.0708 |
| 674.156 | 21.37378 | 674.576 | 35.43382 | 674.394 | 87.76393 | 674.394 | 118.5734 | 674.394 | 194.0663 | 674.394 | 83.6323 | 674.394 | 146.5604 |  | 674.394 | 115.954 |
| 674.886 | 21.15329 | 675.306 | 34.82827 | 675.123 | 86.31111 | 675.123 | 117.0196 | 675.123 | 191.9027 | 675.123 | 81.73481 | 675.123 | 143.9295 |  | 675.123 | 114.7785 |
| 675.615 | 20.91984 | 676.035 | 35.05627 | 675.853 | 83.4288 | 675.853 | 115.6655 | 675.853 | 190.6499 | 675.853 | 80.03651 | 675.853 | 142.2088 |  | 675.853 | 112.1739 |
| 676.342 | 20.67337 | 676.764 | 33.50282 | 676.584 | 80.57246 | 676.584 | 114.2743 | 676.584 | 190.578 | 676.584 | 78.30068 | 676.584 | 141.6683 |  | 676.584 | 109.5956 |
| 677.071 | 20.41576 | 677.494 | 32.47645 | 677.313 | 78.74722 | 677.313 | 112.1724 | 677.313 | 190.5089 | 677.313 | 75.85506 | 677.313 | 141.1318 |  | 677.313 | 108.0476 |
| 677.799 | 20.14787 | 678.223 | 33.99964 | 678.043 | 76.26543 | 678.043 | 110.9601 | 678.043 | 190.5181 | 678.043 | 74.29861 | 678.043 | 140.6732 |  | 678.043 | 105.8435 |
| 678.527 | 19.86639 | 678.952 | 36.03045 | 678.772 | 74.10492 | 678.772 | 108.8181 | 678.772 | 189.7328 | 678.772 | 71.81292 | 678.772 | 139.4205 |  | 678.772 | 103.9603 |
| 679.255 | 19.57141 | 679.682 | 36.62718 | 679.502 | 71.33456 | 679.502 | 107.2896 | 679.502 | 188.0164 | 679.502 | 69.94018 | 679.502 | 137.2361 |  | 679.502 | 101.4676 |
| 679.983 | 19.26392 | 680.411 | 36.22973 | 680.231 | 70.53283 | 680.231 | 105.6959 | 680.231 | 187.2752 | 680.231 | 68.00277 | 680.231 | 136.0277 |  | 680.231 | 100.9432 |
| 680.712 | 18.94591 | 681.139 | 35.66845 | 680.96 | 68.98049 | 680.96 | 103.4447 | 680.96 | 186.127 | 680.96 | 65.40795 | 680.96 | 134.4122 |  | 680.96 | 99.66815 |
| 681.439 | 18.61922 | 681.868 | 35.30973 | 681.689 | 66.97134 | 681.689 | 101.5502 | 681.689 | 184.9304 | 681.689 | 63.16969 | 681.689 | 132.7483 |  | 681.689 | 97.9363 |
| 682.168 | 18.28268 | 682.597 | 34.54436 | 682.419 | 65.32547 | 682.419 | 99.32729 | 682.419 | 183.5244 | 682.419 | 60.60261 | 682.419 | 130.8743 |  | 682.419 | 96.56811 |
| 682.895 | 17.93678 | 683.326 | 35.53145 | 683.147 | 61.77597 | 683.147 | 97.3238 | 683.147 | 181.4097 | 683.147 | 58.25589 | 683.147 | 128.293 |  | 683.147 | 93.29552 |
| 683.623 | 17.58167 | 684.054 | 35.735 | 683.877 | 60.10068 | 683.877 | 96.43177 | 683.877 | 179.9552 | 683.877 | 57.01969 | 683.877 | 126.3705 |  | 683.877 | 91.89792 |
| 684.35 | 17.21807 | 684.784 | 36.46155 | 684.606 | 58.42704 | 684.606 | 96.3843 | 684.606 | 179.3649 | 684.606 | 56.62851 | 684.606 | 125.3129 |  | 684.606 | 90.50157 |
| 685.078 | 16.84532 | 685.512 | 35.65545 | 685.335 | 56.79487 | 685.335 | 94.83247 | 685.335 | 178.5233 | 685.335 | 54.73298 | 685.335 | 124.004 |  | 685.335 | 89.14671 |
| 685.806 | 16.4632 | 686.24 | 34.75673 | 686.064 | 55.57265 | 686.064 | 92.66144 | 686.064 | 176.7408 | 686.064 | 52.21824 | 686.064 | 121.7542 |  | 686.064 | 88.20178 |
| 686.533 | 16.07163 | 686.968 | 34.63809 | 686.792 | 53.74837 | 686.792 | 91.32029 | 686.792 | 174.3898 | 686.792 | 50.53386 | 686.792 | 118.9365 |  | 686.792 | 86.65442 |
| 687.261 | 15.67304 | 687.697 | 35.65464 | 687.521 | 51.36849 | 687.521 | 90.56699 | 687.521 | 172.911 | 687.521 | 49.43685 | 687.521 | 116.9905 |  | 687.521 | 84.55184 |
| 687.987 | 15.27016 | 688.425 | 37.07973 | 688.249 | 48.903 | 688.249 | 90.88668 | 688.249 | 171.2096 | 688.249 | 49.4133 | 688.249 | 114.8223 |  | 688.249 | 82.36326 |
| 688.715 | 14.86547 | 689.153 | 37.36318 | 688.978 | 46.98076 | 688.978 | 90.01249 | 688.978 | 170.0349 | 688.978 | 48.19541 | 688.978 | 113.1804 |  | 688.978 | 80.71833 |
| 689.441 | 14.45886 | 689.882 | 36.83164 | 689.706 | 45.88 | 689.706 | 90.09289 | 689.706 | 169.4197 | 689.706 | 47.93257 | 689.706 | 112.0985 |  | 689.706 | 79.89448 |
| 690.169 | 14.04954 | 690.609 | 37.36055 | 690.435 | 43.3386 | 690.435 | 88.2122 | 690.435 | 167.5659 | 690.435 | 45.70818 | 690.435 | 109.7774 |  | 690.435 | 77.63038 |
| 690.895 | 13.6362 | 691.337 | 34.97909 | 691.163 | 41.22648 | 691.163 | 86.71862 | 691.163 | 166.9874 | 691.163 | 43.87136 | 691.163 | 108.7322 |  | 691.163 | 75.79518 |
| 691.623 | 13.21969 | 692.064 | 33.85355 | 691.892 | 39.68253 | 691.892 | 85.7186 | 691.892 | 165.3208 | 691.892 | 42.52764 | 691.892 | 106.5983 |  | 691.892 | 74.52852 |
| 692.349 | 12.8006 | 692.793 | 33.83255 | 692.619 | 37.01415 | 692.619 | 85.00173 | 692.619 | 164.5385 | 692.619 | 41.46801 | 692.619 | 105.35 |  | 692.619 | 72.13668 |
| 693.076 | 12.37983 | 693.521 | 35.02355 | 693.348 | 33.52646 | 693.348 | 85.35201 | 693.348 | 163.1774 | 693.348 | 41.47457 | 693.348 | 103.5216 |  | 693.348 | 68.92629 |
| 693.802 | 11.96265 | 694.248 | 34.82418 | 694.075 | 31.52749 | 694.075 | 85.45071 | 694.075 | 162.4769 | 694.075 | 41.23052 | 694.075 | 102.3551 |  | 694.075 | 67.20385 |
| 694.529 | 11.54962 | 694.975 | 32.73627 | 694.804 | 29.04178 | 694.804 | 84.71758 | 694.804 | 160.8995 | 694.804 | 40.15368 | 694.804 | 100.3104 |  | 694.804 | 64.99545 |
| 695.255 | 11.14294 | 695.704 | 31.95082 | 695.531 | 26.55776 | 695.531 | 85.85019 | 695.531 | 161.818 | 695.531 | 40.94352 | 695.531 | 100.7629 |  | 695.531 | 62.78796 |
| 695.982 | 10.74592 | 696.431 | 31.22245 | 696.258 | 23.72127 | 696.258 | 85.23879 | 696.258 | 161.6182 | 696.258 | 39.98936 | 696.258 | 100.097 |  | 696.258 | 60.22801 |
| 696.708 | 10.36325 | 697.158 | 31.696 | 696.986 | 22.58313 | 696.986 | 84.09097 | 696.986 | 159.9426 | 696.986 | 38.49831 | 696.986 | 97.9548 |  | 696.986 | 59.36679 |
| 697.435 | 9.99584 | 697.885 | 31.32873 | 697.713 | 21.21232 | 697.713 | 83.60398 | 697.713 | 160.4955 | 697.713 | 37.66855 | 697.713 | 98.04168 |  | 697.713 | 58.27252 |
| 698.16 | 9.6449 | 698.611 | 31.46355 | 698.442 | 19.42089 | 698.442 | 82.22656 | 698.442 | 161.7645 | 698.442 | 35.94743 | 698.442 | 98.84339 |  | 698.442 | 56.75838 |
| 698.887 | 9.31369 | 699.34 | 33.51945 | 699.168 | 17.14715 | 699.168 | 79.47236 | 699.168 | 160.7721 | 699.168 | 32.85094 | 699.168 | 97.38557 |  | 699.168 | 54.7608 |
| 699.612 | 9.00325 | 700.066 | 34.25909 | 699.896 | 15.25197 | 699.896 | 78.23692 | 699.896 | 160.1742 | 699.896 | 31.27226 | 699.896 | 96.32099 |  | 699.896 | 53.14254 |
| 700.339 | 8.714 | 700.793 | 34.16718 | 700.623 | 13.83081 | 700.623 | 77.03744 | 700.623 | 159.351 | 700.623 | 29.73002 | 700.623 | 95.03181 |  | 700.623 | 51.99792 |
| 701.064 | 8.44629 | 701.52 | 32.88836 | 701.351 | 11.67193 | 701.351 | 77.06663 | 701.351 | 158.2733 | 701.351 | 29.41598 | 701.351 | 93.48743 |  | 701.351 | 50.11596 |
| 701.791 | 8.20341 | 702.247 | 34.66236 | 702.078 | 9.96293 | 702.078 | 77.46802 | 702.078 | 157.1654 | 702.078 | 29.4746 | 702.078 | 91.91353 |  | 702.078 | 48.68349 |
| 702.516 | 7.98651 | 702.974 | 35.578 | 702.806 | 9.65227 | 702.806 | 77.21338 | 702.806 | 156.3691 | 702.806 | 28.87673 | 702.806 | 90.65051 |  | 702.806 | 48.64975 |
| 703.242 | 7.79564 | 703.7 | 34.09818 | 703.532 | 8.88132 | 703.532 | 77.1407 | 703.532 | 156.895 | 703.532 | 28.46176 | 703.532 | 90.71112 |  | 703.532 | 48.15495 |
| 703.967 | 7.63107 | 704.427 | 33.56773 | 704.258 | 7.41912 | 704.258 | 77.52254 | 704.258 | 156.5888 | 704.258 | 28.50131 | 704.258 | 89.93951 |  | 704.258 | 46.96892 |
| 704.692 | 7.49282 | 705.153 | 32.49582 | 704.986 | 5.88056 | 704.986 | 78.21525 | 704.986 | 156.0351 | 704.986 | 28.85078 | 704.986 | 88.91915 |  | 704.986 | 45.70727 |
| 705.419 | 7.38076 | 705.88 | 33.20991 | 705.712 | 4.46971 | 705.712 | 79.11596 | 705.712 | 154.3124 | 705.712 | 29.4092 | 705.712 | 86.73103 |  | 705.712 | 44.57258 |
| 706.143 | 7.29497 | 706.606 | 33.08236 | 706.44 | 2.96019 | 706.44 | 79.0888 | 706.44 | 154.0295 | 706.44 | 29.0388 | 706.44 | 85.98146 |  | 706.44 | 43.33998 |
| 706.869 | 7.23326 | 707.333 | 33.974 | 707.166 | 2.67286 | 707.166 | 78.69293 | 707.166 | 154.384 | 707.166 | 28.30064 | 707.166 | 85.87058 |  | 707.166 | 43.3288 |
| 707.594 | 7.19529 | 708.058 | 33.89673 | 707.893 | 3.43862 | 707.893 | 78.42695 | 707.893 | 155.0451 | 707.893 | 27.6919 | 707.893 | 86.06571 |  | 707.893 | 44.3711 |
| 708.32 | 7.18141 | 708.784 | 33.67509 | 708.619 | 3.278 | 708.619 | 77.99929 | 708.619 | 154.7861 | 708.619 | 26.92195 | 708.619 | 85.34133 |  | 708.619 | 44.48664 |
| 709.044 | 7.1926 | 709.51 | 33.48782 | 709.345 | 3.14669 | 709.345 | 78.6892 | 709.345 | 155.3082 | 709.345 | 27.26957 | 709.345 | 85.398 |  | 709.345 | 44.63148 |
| 709.77 | 7.22618 | 710.237 | 32.92818 | 710.072 | 2.97686 | 710.072 | 79.63739 | 710.072 | 156.0945 | 710.072 | 27.875 | 710.072 | 85.71831 |  | 710.072 | 44.73819 |
| 710.494 | 7.28019 | 710.963 | 33.12236 | 710.797 | 2.74813 | 710.797 | 78.70289 | 710.797 | 158.196 | 710.797 | 26.59867 | 710.797 | 87.35503 |  | 710.797 | 44.78524 |
| 711.219 | 7.35435 | 711.689 | 33.42391 | 711.525 | 2.70871 | 711.525 | 78.75203 | 711.525 | 158.7319 | 711.525 | 26.30458 | 711.525 | 87.42434 |  | 711.525 | 45.02273 |
| 711.944 | 7.44655 | 712.414 | 33.68527 | 712.25 | 1.17095 | 712.25 | 79.55153 | 712.25 | 159.5906 | 712.25 | 26.76226 | 712.25 | 87.81829 |  | 712.25 | 43.76075 |
| 712.668 | 7.55722 | 713.14 | 34.48745 | 712.976 | 0.6292 | 712.976 | 79.66108 | 712.976 | 159.2491 | 712.976 | 26.52952 | 712.976 | 87.01137 |  | 712.976 | 43.49516 |
| 713.394 | 7.68529 | 713.865 | 34.09355 | 713.702 | 0.62363 | 713.702 | 80.56373 | 713.702 | 158.6829 | 713.702 | 27.08988 | 713.702 | 85.97984 |  | 713.702 | 43.76575 |
| 714.118 | 7.82947 | 714.592 | 33.918 | 714.428 | -0.16244 | 714.428 | 81.10239 | 714.428 | 159.8947 | 714.428 | 27.28624 | 714.428 | 86.72623 |  | 714.428 | 43.25583 |
| 714.842 | 7.99025 | 715.317 | 32.59109 | 715.154 | -0.19608 | 715.154 | 80.93881 | 715.154 | 159.1371 | 715.154 | 26.78037 | 715.154 | 85.50329 |  | 715.154 | 43.49835 |
| 715.567 | 8.16928 | 716.042 | 32.50882 | 715.88 | 0.16194 | 715.88 | 81.64583 | 715.88 | 159.1862 | 715.88 | 27.1451 | 715.88 | 85.08694 |  | 715.88 | 43.99297 |
| 716.291 | 8.36764 | 716.767 | 32.51809 | 716.605 | 1.50306 | 716.605 | 81.98971 | 716.605 | 160.0881 | 716.605 | 27.14716 | 716.605 | 85.52418 |  | 716.605 | 44.2494 |
| 717.016 | 8.583 | 717.492 | 32.662 | 717.331 | 1.3776 | 717.331 | 80.3247 | 717.331 | 161.407 | 717.331 | 25.13986 | 717.331 | 86.37765 |  | 717.331 | 43.03777 |
| 717.739 | 8.81429 | 718.217 | 32.48845 | 718.056 | 1.5468 | 718.056 | 81.10895 | 718.056 | 163.1098 | 718.056 | 25.58229 | 718.056 | 87.6157 |  | 718.056 | 42.12229 |
| 718.463 | 9.06015 | 718.942 | 31.60345 | 718.781 | 2.1257 | 718.781 | 82.27155 | 718.781 | 163.6444 | 718.781 | 26.40308 | 718.781 | 87.6856 |  | 718.781 | 41.6165 |
| 719.188 | 9.31218 | 719.667 | 32.40455 | 719.507 | 3.06385 | 719.507 | 82.69087 | 719.507 | 164.3161 | 719.507 | 26.4801 | 719.507 | 87.89187 |  | 719.507 | 41.46847 |
| 719.911 | 9.56635 | 720.393 | 31.66891 | 720.232 | 5.54867 | 720.232 | 82.94835 | 720.232 | 164.5372 | 720.232 | 26.39576 | 720.232 | 87.64828 |  | 720.232 | 42.86862 |
| 720.636 | 9.8226 | 721.118 | 32.30136 | 720.958 | 6.5051 | 720.958 | 83.04117 | 720.958 | 165.0034 | 720.958 | 26.14629 | 720.958 | 87.6491 |  | 720.958 | 42.73887 |
| 721.359 | 10.07976 | 721.842 | 32.75964 | 721.683 | 7.90701 | 721.683 | 81.46917 | 721.683 | 165.0628 | 721.683 | 24.23247 | 721.683 | 87.24374 |  | 721.683 | 43.05609 |
| 722.083 | 10.33513 | 722.567 | 31.22845 | 722.407 | 8.55829 | 722.407 | 81.05447 | 722.407 | 165.1916 | 722.407 | 23.47642 | 722.407 | 86.90847 |  | 722.407 | 42.62419 |
| 722.807 | 10.58743 | 723.291 | 32.20827 | 723.133 | 9.83911 | 723.133 | 81.44985 | 723.133 | 166.3493 | 723.133 | 23.52951 | 723.133 | 87.60072 |  | 723.133 | 42.81883 |
| 723.53 | 10.83479 | 724.016 | 30.66936 | 723.858 | 10.49364 | 723.858 | 81.36689 | 723.858 | 166.9442 | 723.858 | 23.10473 | 723.858 | 87.73092 |  | 723.858 | 42.38868 |
| 724.253 | 11.07524 | 724.74 | 32.02482 | 724.582 | 10.91793 | 724.582 | 81.42377 | 724.582 | 167.4937 | 724.582 | 22.82026 | 724.582 | 87.81629 |  | 724.582 | 41.72979 |
| 724.977 | 11.30778 | 725.464 | 33.83736 | 725.308 | 12.47401 | 725.308 | 80.92693 | 725.308 | 168.4203 | 725.308 | 21.98113 | 725.308 | 88.27751 |  | 725.308 | 42.19969 |
| 725.7 | 11.52925 | 726.189 | 33.389 | 726.032 | 13.55365 | 726.032 | 80.79888 | 726.032 | 168.4833 | 726.032 | 21.51173 | 726.032 | 87.87644 |  | 726.032 | 42.19614 |
| 726.423 | 11.73741 | 726.914 | 34.392 | 726.756 | 13.78986 | 726.756 | 80.0361 | 726.756 | 168.4555 | 726.756 | 20.4076 | 726.756 | 87.3845 |  | 726.756 | 41.34917 |
| 727.147 | 11.93236 | 727.638 | 33.85309 | 727.482 | 14.7217 | 727.482 | 80.2632 | 727.482 | 167.8056 | 727.482 | 20.29241 | 727.482 | 86.26931 |  | 727.482 | 41.19483 |
| 727.87 | 12.11441 | 728.362 | 33.31827 | 728.206 | 14.97184 | 728.206 | 79.42755 | 728.206 | 166.8341 | 728.206 | 19.11541 | 728.206 | 84.83363 |  | 728.206 | 40.36178 |
| 728.593 | 12.28137 | 729.086 | 31.56936 | 728.93 | 14.82877 | 728.93 | 77.84917 | 728.93 | 166.9553 | 728.93 | 17.19569 | 728.93 | 84.49082 |  | 728.93 | 39.13553 |
| 729.316 | 12.43295 | 729.81 | 30.31255 | 729.655 | 16.03278 | 729.655 | 77.25198 | 729.655 | 166.0215 | 729.655 | 16.25667 | 729.655 | 83.09221 |  | 729.655 | 39.25485 |
| 730.039 | 12.56897 | 730.534 | 32.09045 | 730.379 | 16.96245 | 730.379 | 75.87192 | 730.379 | 166.8916 | 730.379 | 14.53526 | 730.379 | 83.4982 |  | 730.379 | 39.10134 |
| 730.761 | 12.68864 | 731.258 | 32.10791 | 731.102 | 17.03679 | 731.102 | 73.96328 | 731.102 | 166.436 | 731.102 | 12.28574 | 731.102 | 82.57918 |  | 731.102 | 38.09399 |
| 731.485 | 12.79292 | 731.981 | 33.197 | 731.827 | 17.34361 | 731.827 | 72.27496 | 731.827 | 165.5793 | 731.827 | 10.2556 | 731.827 | 81.25771 |  | 731.827 | 37.31613 |
| 732.207 | 12.88282 | 732.705 | 31.46691 | 732.551 | 17.23981 | 732.551 | 69.78319 | 732.551 | 162.9453 | 732.551 | 7.42249 | 732.551 | 78.15968 |  | 732.551 | 36.12914 |
| 732.929 | 12.9574 | 733.428 | 31.09436 | 733.275 | 18.49529 | 733.275 | 69.86684 | 733.275 | 162.4755 | 733.275 | 7.16479 | 733.275 | 77.22579 |  | 733.275 | 36.30144 |
| 733.653 | 13.01668 | 734.152 | 32.00791 | 733.998 | 18.46368 | 733.998 | 69.70222 | 733.998 | 162.103 | 733.998 | 6.65929 | 733.998 | 76.38982 |  | 733.998 | 35.18813 |
| 734.375 | 13.06133 | 734.875 | 32.01327 | 734.723 | 17.5624 | 734.723 | 68.0994 | 734.723 | 160.7998 | 734.723 | 4.71465 | 734.723 | 74.6218 |  | 734.723 | 33.20217 |
| 735.097 | 13.09399 | 735.599 | 32.29109 | 735.446 | 17.79073 | 735.446 | 67.22741 | 735.446 | 159.8254 | 735.446 | 3.50178 | 735.446 | 73.18403 |  | 735.446 | 32.34881 |
| 735.82 | 13.11609 | 736.322 | 33.98082 | 736.169 | 18.1266 | 736.169 | 67.92039 | 736.169 | 160.635 | 736.169 | 3.85389 | 736.169 | 73.53011 |  | 736.169 | 31.60299 |
| 736.542 | 13.12868 | 737.045 | 34.36145 | 736.894 | 18.7408 | 736.894 | 67.52763 | 736.894 | 161.423 | 736.894 | 3.11931 | 736.894 | 73.85344 |  | 736.894 | 31.13251 |
| 737.264 | 13.13254 | 737.768 | 35.51055 | 737.617 | 19.78246 | 737.617 | 66.47001 | 737.617 | 161.7799 | 737.617 | 1.72081 | 737.617 | 73.74682 |  | 737.617 | 31.09248 |
| 737.985 | 13.12833 | 738.492 | 35.343 | 738.34 | 20.51421 | 738.34 | 65.81913 | 738.34 | 161.1009 | 738.34 | 0.72905 | 738.34 | 72.60444 |  | 738.34 | 30.74254 |
| 738.708 | 13.11596 | 739.215 | 34.09736 | 739.063 | 21.2619 | 739.063 | 64.37102 | 739.063 | 160.9255 | 739.063 | -1.05993 | 739.063 | 71.96548 |  | 739.063 | 30.40854 |
| 739.43 | 13.09641 | 739.938 | 34.00536 | 739.787 | 20.77785 | 739.787 | 63.39327 | 739.787 | 161.3833 | 739.787 | -2.37903 | 739.787 | 71.9592 |  | 739.787 | 28.8413 |
| 740.151 | 13.07042 | 740.661 | 34.54291 | 740.51 | 20.42391 | 740.51 | 62.54384 | 740.51 | 160.0246 | 740.51 | -3.56933 | 740.51 | 70.13703 |  | 740.51 | 27.40567 |
| 740.874 | 13.03886 | 741.384 | 34.10427 | 741.233 | 21.13314 | 741.233 | 61.71618 | 741.233 | 158.1296 | 741.233 | -4.73788 | 741.233 | 67.77865 |  | 741.233 | 27.03322 |
| 741.596 | 13.00218 | 742.107 | 33.90609 | 741.957 | 21.04102 | 741.957 | 60.8167 | 741.957 | 157.9172 | 741.957 | -5.9787 | 741.957 | 67.10217 |  | 741.957 | 25.85791 |
| 742.317 | 12.96003 | 742.829 | 32.62427 | 742.68 | 21.25237 | 742.68 | 59.8911 | 742.68 | 158.9427 | 742.68 | -7.24519 | 742.68 | 67.66421 |  | 742.68 | 24.98757 |
| 743.038 | 12.91259 | 743.552 | 33.25609 | 743.402 | 21.83598 | 743.402 | 59.37896 | 743.402 | 158.8607 | 743.402 | -8.09773 | 743.402 | 67.11931 |  | 743.402 | 24.49099 |
| 743.761 | 12.86049 | 744.274 | 31.58845 | 744.125 | 21.6604 | 744.125 | 58.95403 | 744.125 | 157.5682 | 744.125 | -8.86354 | 744.125 | 65.36335 |  | 744.125 | 23.23372 |
| 744.482 | 12.80433 | 744.997 | 32.29318 | 744.848 | 20.82877 | 744.848 | 58.36652 | 744.848 | 155.9022 | 744.848 | -9.79193 | 744.848 | 63.23389 |  | 744.848 | 21.3204 |
| 745.203 | 12.74511 | 745.719 | 32.452 | 745.571 | 20.66227 | 745.571 | 57.60095 | 745.571 | 155.1311 | 745.571 | -10.8984 | 745.571 | 61.9994 |  | 745.571 | 20.0722 |
| 745.924 | 12.68438 | 746.441 | 32.20091 | 746.293 | 19.66338 | 746.293 | 56.68659 | 746.293 | 152.8186 | 746.293 | -12.1531 | 746.293 | 59.2241 |  | 746.293 | 17.99313 |
| 746.646 | 12.62281 | 747.163 | 31.47645 | 747.015 | 19.19532 | 747.015 | 54.78692 | 747.015 | 150.208 | 747.015 | -14.3932 | 747.015 | 56.15063 |  | 747.015 | 16.44487 |
| 747.367 | 12.56059 | 747.885 | 31.21864 | 747.737 | 18.90945 | 747.737 | 54.56197 | 747.737 | 148.2429 | 747.737 | -14.9586 | 747.737 | 53.72278 |  | 747.737 | 15.07881 |
| 748.087 | 12.49766 | 748.607 | 31.73927 | 748.461 | 19.02311 | 748.461 | 53.5327 | 748.461 | 145.3289 | 748.461 | -16.3292 | 748.461 | 50.34463 |  | 748.461 | 14.10929 |
| 748.808 | 12.43465 | 749.329 | 29.83409 | 749.183 | 19.26989 | 749.183 | 52.52816 | 749.183 | 142.9834 | 749.183 | -17.6741 | 749.183 | 47.53635 |  | 749.183 | 13.27587 |
| 749.53 | 12.37342 | 750.051 | 29.365 | 749.905 | 18.87276 | 749.905 | 51.83965 | 749.905 | 141.35 | 749.905 | -18.703 | 749.905 | 45.44008 |  | 749.905 | 11.79854 |
| 750.251 | 12.31506 | 750.773 | 29.77273 | 750.627 | 18.25452 | 750.627 | 49.98885 | 750.627 | 139.2396 | 750.627 | -20.8943 | 750.627 | 42.86689 |  | 750.627 | 10.10011 |
| 750.971 | 12.26042 | 751.495 | 29.08518 | 751.35 | 18.10526 | 751.35 | 49.63108 | 751.35 | 136.7276 | 751.35 | -21.5929 | 751.35 | 39.89147 |  | 751.35 | 8.86917 |
| 751.691 | 12.20873 | 752.217 | 30.10209 | 752.072 | 17.20299 | 752.072 | 48.7156 | 752.072 | 135.3008 | 752.072 | -22.8488 | 752.072 | 38.00186 |  | 752.072 | 6.88669 |
| 752.412 | 12.16061 | 752.938 | 29.30091 | 752.793 | 16.55315 | 752.793 | 47.39178 | 752.793 | 132.9817 | 752.793 | -24.5125 | 752.793 | 35.22057 |  | 752.793 | 5.15816 |
| 753.133 | 12.11418 | 753.66 | 29.61073 | 753.515 | 16.58037 | 753.515 | 45.88792 | 753.515 | 130.4742 | 753.515 | -26.3568 | 753.515 | 32.25027 |  | 753.515 | 4.10519 |
| 753.853 | 12.06972 | 754.38 | 29.53036 | 754.236 | 16.14337 | 754.236 | 44.76651 | 754.236 | 128.027 | 754.236 | -27.8181 | 754.236 | 29.34084 |  | 754.236 | 2.58949 |
| 754.574 | 12.02807 | 755.102 | 30.13209 | 754.959 | 15.73251 | 754.959 | 43.52423 | 754.959 | 125.2032 | 754.959 | -29.4013 | 754.959 | 26.05361 |  | 754.959 | 1.09694 |
| 755.294 | 11.99035 | 755.823 | 31.01345 | 755.681 | 15.40649 | 755.681 | 41.74428 | 755.681 | 121.7762 | 755.681 | -31.5217 | 755.681 | 22.16379 |  | 755.681 | -0.30927 |
| 756.014 | 11.95729 | 756.544 | 29.75427 | 756.402 | 14.21448 | 756.402 | 40.90245 | 756.402 | 119.4932 | 756.402 | -32.7034 | 756.402 | 19.41856 |  | 756.402 | -2.57998 |
| 756.735 | 11.92997 | 757.265 | 30.99291 | 757.123 | 13.00229 | 757.123 | 40.0273 | 757.123 | 117.9732 | 757.123 | -33.9185 | 757.123 | 17.43643 |  | 757.123 | -4.87086 |
| 757.455 | 11.90828 | 757.987 | 31.32445 | 757.844 | 12.60444 | 757.844 | 38.66917 | 757.844 | 113.841 | 757.844 | -35.6166 | 757.844 | 12.84203 |  | 757.844 | -6.34742 |
| 758.174 | 11.89237 | 758.708 | 32.93745 | 758.567 | 12.36884 | 758.567 | 38.88987 | 758.567 | 110.0035 | 758.567 | -35.7367 | 758.567 | 8.54113 |  | 758.567 | -7.66471 |
| 758.894 | 11.8835 | 759.429 | 34.38345 | 759.288 | 11.92066 | 759.288 | 37.48316 | 759.288 | 107.235 | 759.288 | -37.4834 | 759.288 | 5.31038 |  | 759.288 | -9.19158 |
| 759.614 | 11.88353 | 760.15 | 34.18691 | 760.009 | 9.87623 | 760.009 | 35.27841 | 760.009 | 103.5267 | 760.009 | -40.0281 | 760.009 | 1.13997 |  | 760.009 | -12.3147 |
| 760.335 | 11.8928 | 760.87 | 33.59509 | 760.73 | 9.0187 | 760.73 | 33.2776 | 760.73 | 100.5398 | 760.73 | -42.3688 | 760.73 | -2.30914 |  | 760.73 | -14.2509 |
| 761.054 | 11.91204 | 761.591 | 31.92164 | 761.45 | 9.45185 | 761.45 | 31.68805 | 761.45 | 98.43993 | 761.45 | -44.2978 | 761.45 | -4.87052 |  | 761.45 | -14.895 |
| 761.774 | 11.94406 | 762.312 | 31.70255 | 762.171 | 7.90688 | 762.171 | 29.71109 | 762.171 | 95.08811 | 762.171 | -46.6147 | 762.171 | -8.68452 |  | 762.171 | -17.5187 |
| 762.493 | 11.99054 | 763.033 | 30.14264 | 762.893 | 6.41598 | 762.893 | 27.24911 | 762.893 | 92.36726 | 762.893 | -49.4171 | 762.893 | -11.8682 |  | 762.893 | -20.0898 |
| 763.212 | 12.05158 | 763.753 | 29.76209 | 763.614 | 6.09536 | 763.614 | 25.93195 | 763.614 | 90.68964 | 763.614 | -51.0742 | 763.614 | -14.008 |  | 763.614 | -21.4891 |
| 763.931 | 12.13002 | 764.474 | 30.43691 | 764.334 | 5.88073 | 764.334 | 23.70001 | 764.334 | 88.69074 | 764.334 | -53.6456 | 764.334 | -16.4684 |  | 764.334 | -22.7809 |
| 764.651 | 12.22797 | 765.193 | 29.67055 | 765.055 | 5.4615 | 765.055 | 22.75085 | 765.055 | 85.86946 | 765.055 | -54.9347 | 765.055 | -19.7519 |  | 765.055 | -24.2788 |
| 765.371 | 12.34665 | 765.913 | 27.20436 | 765.775 | 5.10843 | 765.775 | 22.17513 | 765.775 | 83.10652 | 765.775 | -55.8499 | 765.775 | -22.9763 |  | 765.775 | -25.7091 |
| 766.09 | 12.48761 | 766.634 | 24.59955 | 766.496 | 3.27097 | 766.496 | 20.1863 | 766.496 | 80.44004 | 766.496 | -58.1787 | 766.496 | -26.105 |  | 766.496 | -28.6253 |
| 766.809 | 12.6521 | 767.354 | 22.31364 | 767.217 | 2.73728 | 767.217 | 20.18911 | 767.217 | 76.75632 | 767.217 | -58.5158 | 767.217 | -30.2509 |  | 767.217 | -30.2376 |
| 767.528 | 12.84126 | 768.074 | 21.66591 | 767.938 | 2.42399 | 767.938 | 19.29129 | 767.938 | 73.32193 | 767.938 | -59.7535 | 767.938 | -34.1475 |  | 767.938 | -31.6296 |
| 768.247 | 13.05642 | 768.794 | 22.35191 | 768.658 | 2.23687 | 768.658 | 18.42572 | 768.658 | 70.99687 | 768.658 | -60.9586 | 768.658 | -36.934 |  | 768.658 | -32.894 |
| 768.965 | 13.29716 | 769.514 | 22.30791 | 769.378 | 2.26821 | 769.378 | 17.02482 | 769.378 | 68.90743 | 769.378 | -62.6989 | 769.378 | -39.485 |  | 769.378 | -33.9398 |
| 769.684 | 13.56296 | 770.234 | 21.17209 | 770.098 | 1.53526 | 770.098 | 15.34473 | 770.098 | 65.09587 | 770.098 | -64.7185 | 770.098 | -43.7581 |  | 770.098 | -35.75 |
| 770.404 | 13.85152 | 770.954 | 22.07918 | 770.818 | -0.2451 | 770.818 | 14.09827 | 770.818 | 59.95118 | 770.818 | -66.3044 | 770.818 | -49.3643 |  | 770.818 | -38.6075 |
| 771.122 | 14.16169 | 771.674 | 20.40845 | 771.537 | -0.47714 | 771.537 | 13.84651 | 771.537 | 56.84639 | 771.537 | -66.8952 | 771.537 | -52.93 |  | 771.537 | -39.9153 |
| 771.841 | 14.49103 | 772.392 | 17.99491 | 772.257 | -1.94902 | 772.257 | 12.60865 | 772.257 | 53.29106 | 772.257 | -68.4725 | 772.257 | -56.9469 |  | 772.257 | -42.4644 |
| 772.559 | 14.83708 | 773.112 | 18.61591 | 772.978 | -3.09232 | 772.978 | 10.84997 | 772.978 | 48.3777 | 772.978 | -70.5711 | 772.978 | -62.3224 |  | 772.978 | -44.6864 |
| 773.278 | 15.1969 | 773.832 | 19.24073 | 773.698 | -4.33121 | 773.698 | 9.56054 | 773.698 | 43.29944 | 773.698 | -72.2 | 773.698 | -67.8622 |  | 773.698 | -47.0024 |
| 773.996 | 15.56862 | 774.551 | 19.54764 | 774.418 | -5.05869 | 774.418 | 9.87612 | 774.418 | 39.60333 | 774.418 | -72.2239 | 774.418 | -72.0199 |  | 774.418 | -48.8071 |
| 774.714 | 15.95028 | 775.271 | 20.99064 | 775.137 | -5.48805 | 775.137 | 9.14147 | 775.137 | 37.80198 | 775.137 | -73.2975 | 775.137 | -74.2821 |  | 775.137 | -50.3122 |
| 775.432 | 16.34025 | 775.99 | 21.26155 | 775.857 | -5.93334 | 775.857 | 8.68971 | 775.857 | 36.00847 | 775.857 | -74.0887 | 775.857 | -76.5371 |  | 775.857 | -51.8347 |
| 776.15 | 16.7359 | 776.71 | 20.12318 | 776.576 | -5.24324 | 776.576 | 8.04541 | 776.576 | 32.90683 | 776.576 | -75.072 | 776.576 | -80.0997 |  | 776.576 | -52.2203 |
| 776.869 | 17.13417 | 777.427 | 19.57082 | 777.295 | -4.66369 | 777.295 | 7.24105 | 777.295 | 29.03567 | 777.295 | -76.2154 | 777.295 | -84.4317 |  | 777.295 | -52.7164 |
| 777.587 | 17.53328 | 778.147 | 19.025 | 778.014 | -4.56313 | 778.014 | 6.64226 | 778.014 | 26.38133 | 778.014 | -77.1532 | 778.014 | -87.547 |  | 778.014 | -53.6916 |
| 778.305 | 17.93207 | 778.866 | 18.792 | 778.734 | -4.63498 | 778.734 | 5.31973 | 778.734 | 23.51724 | 778.734 | -78.8151 | 778.734 | -90.8726 |  | 778.734 | -54.8406 |
| 779.023 | 18.32854 | 779.585 | 18.88564 | 779.454 | -4.81974 | 779.454 | 4.43825 | 779.454 | 19.08487 | 779.454 | -80.0361 | 779.454 | -95.7665 |  | 779.454 | -56.1026 |
| 779.741 | 18.72037 | 780.304 | 19.79255 | 780.173 | -5.33205 | 780.173 | 3.08167 | 780.173 | 15.23318 | 780.173 | -81.7317 | 780.173 | -100.079 |  | 780.173 | -57.6906 |
| 780.458 | 19.10732 | 781.023 | 19.242 | 780.892 | -5.24669 | 780.892 | 2.39499 | 780.892 | 12.84992 | 780.892 | -82.7573 | 780.892 | -102.923 |  | 780.892 | -58.681 |
| 781.176 | 19.48921 | 781.74 | 20.58782 | 781.611 | -4.73757 | 781.611 | 2.14824 | 781.611 | 11.16554 | 781.611 | -83.3431 | 781.611 | -105.069 |  | 781.611 | -59.2475 |
| 781.893 | 19.86446 | 782.459 | 19.98855 | 782.33 | -3.72391 | 782.33 | 1.74904 | 782.33 | 8.62351 | 782.33 | -84.0813 | 782.33 | -108.071 |  | 782.33 | -59.3096 |
| 782.611 | 20.08968 | 783.178 | 17.52245 | 783.049 | -1.54553 | 783.049 | 1.71694 | 783.049 | 5.51707 | 783.049 | -84.4524 | 783.049 | -111.639 |  | 783.049 | -58.2069 |
| 783.328 | 20.31137 | 783.897 | 18.04527 | 783.767 | -1.15763 | 783.767 | 1.27977 | 783.767 | 3.79725 | 783.767 | -85.228 | 783.767 | -113.819 |  | 783.767 | -58.8932 |
| 784.045 | 20.5296 | 784.615 | 18.14218 | 784.486 | -1.35507 | 784.486 | 1.06594 | 784.486 | 2.31773 | 784.486 | -85.7809 | 784.486 | -115.759 |  | 784.486 | -60.1664 |
| 784.763 | 20.7442 | 785.334 | 19.24727 | 785.204 | -2.02672 | 785.204 | 1.18664 | 785.204 | 2.21658 | 785.204 | -85.9987 | 785.204 | -116.321 |  | 785.204 | -61.9122 |
| 785.48 | 20.95533 | 786.051 | 20.40727 | 785.923 | -1.24351 | 785.923 | 0.62967 | 785.923 | 0 | 785.923 | -86.8946 | 785.923 | -118.998 |  | 785.923 | -62.2047 |
| 786.197 | 21.16335 | 786.769 | 20.53845 | 786.641 | 0 | 786.641 | 0 | 786.641 | -1.49147 | 786.641 | -87.8628 | 786.641 | -120.238 |  | 786.641 | -62.0354 |
| 786.914 | 21.36834 | 787.488 | 20.32045 | 787.36 | 0.16626 | 787.36 | -1.14382 | 787.36 | -3.36001 | 787.36 | -88.5251 | 787.36 | -121.854 |  | 787.36 | -61.2863 |
| 787.631 | 21.57044 | 788.206 | 20.11145 | 788.078 | -0.80469 | 788.078 | -3.12651 | 788.078 | -6.16472 | 788.078 | -90.0268 | 788.078 | -124.407 |  | 788.078 | -61.6752 |
| 788.348 | 21.76975 | 788.924 | 19.252 | 788.796 | -1.56777 | 788.796 | -4.24635 | 788.796 | -7.26531 | 788.796 | -90.6658 | 788.796 | -125.256 |  | 788.796 | -61.8562 |
| 789.066 | 21.96643 | 789.641 | 16.88718 | 789.514 | -2.50768 | 789.514 | -5.25551 | 789.514 | -7.80609 | 789.514 | -91.194 | 789.514 | -125.545 |  | 789.514 | -62.214 |
| 789.783 | 22.16033 | 790.359 | 16.34391 | 790.232 | -4.07366 | 790.232 | -6.3754 | 790.232 | -9.79814 | 790.232 | -91.833 | 790.232 | -127.286 |  | 790.232 | -63.198 |
| 790.499 | 22.35137 | 791.077 | 16.77745 | 790.95 | -4.31509 | 790.95 | -6.12264 | 790.95 | -10.5908 | 790.95 | -91.0993 | 790.95 | -127.827 |  | 790.95 | -62.8573 |
| 791.216 | 22.53991 | 791.795 | 16.59 | 791.668 | -5.12336 | 791.668 | -5.22114 | 791.668 | -13.2181 | 791.668 | -89.7169 | 791.668 | -130.202 |  | 791.668 | -63.0835 |
| 791.932 | 22.72599 | 792.511 | 16.66282 | 792.386 | -5.00042 | 792.386 | -4.88129 | 792.386 | -13.4534 | 792.386 | -88.8961 | 792.386 | -130.186 |  | 792.386 | -62.3785 |
| 792.649 | 22.90964 | 793.229 | 14.40373 | 793.105 | -3.97728 | 793.105 | -4.89457 | 793.105 | -14.5472 | 793.105 | -88.4278 | 793.105 | -131.028 |  | 793.105 | -60.7725 |
| 793.365 | 23.0911 | 793.947 | 14.53009 | 793.823 | -2.95507 | 793.823 | -5.12868 | 793.823 | -14.8772 | 793.823 | -88.181 | 793.823 | -131.106 |  | 793.823 | -59.1683 |
| 794.082 | 23.27052 | 794.664 | 13.28645 | 794.541 | -3.20872 | 794.541 | -4.79817 | 794.541 | -14.3822 | 794.541 | -87.3695 | 794.541 | -130.359 |  | 794.541 | -58.8398 |
| 794.798 | 23.44826 | 795.382 | 13.41182 | 795.258 | -2.72879 | 795.258 | -5.49476 | 795.258 | -14.6116 | 795.258 | -87.5859 | 795.258 | -130.337 |  | 795.258 | -57.7787 |
| 795.514 | 23.62415 | 796.098 | 14.078 | 795.976 | -2.45906 | 795.976 | -4.6647 | 795.976 | -14.5379 | 795.976 | -86.2749 | 795.976 | -130.012 |  | 795.976 | -56.9269 |
| 796.23 | 23.79847 | 796.816 | 14.21682 | 796.693 | -1.04987 | 796.693 | -3.48252 | 796.693 | -14.7313 | 796.693 | -84.6125 | 796.693 | -129.954 |  | 796.693 | -54.9364 |
| 796.469 | 23.97133 | 797.533 | 15.339 | 797.411 | -0.76381 | 797.411 | -2.58012 | 797.411 | -14.3149 | 797.411 | -83.2291 | 797.411 | -129.286 |  | 797.411 | -54.0683 |
| 797.187 | 24.14312 | 798.25 | 14.84973 | 798.128 | 0.0731 | 798.128 | -1.65887 | 798.128 | -15.2182 | 798.128 | -81.8276 | 798.128 | -129.938 |  | 798.128 | -52.6502 |
| 797.905 | 24.31388 | 798.966 | 14.757 | 798.845 | 1.21944 | 798.845 | 0.12346 | 798.845 | -15.2932 | 798.845 | -79.565 | 798.845 | -129.761 |  | 798.845 | -50.9226 |
| 798.623 | 24.48374 | 799.683 | 13.20055 | 799.562 | 2.05444 | 799.562 | 1.73607 | 799.562 | -15.0952 | 799.562 | -77.4722 | 799.562 | -129.312 |  | 799.562 | -49.5063 |
| 799.341 | 24.65285 | 800.4 | 11.51673 | 800.279 | 2.84378 | 800.279 | 2.707 | 800.279 | -14.3776 | 800.279 | -76.021 | 800.279 | -128.343 |  | 800.279 | -48.1357 |
| 800.058 | 24.82141 | 801.117 | 13.83191 | 800.997 | 2.75508 | 800.997 | 4.01244 | 800.997 | -14.1015 | 800.997 | -74.2346 | 800.997 | -127.815 |  | 800.997 | -47.6424 |
| 800.777 | 24.9895 | 801.833 | 14.43727 | 801.714 | 4.13505 | 801.714 | 5.70983 | 801.714 | -14.0216 | 801.714 | -72.057 | 801.714 | -127.484 |  | 801.714 | -45.6811 |
| 801.494 | 25.1571 | 802.55 | 14.85264 | 802.429 | 5.99295 | 802.429 | 6.05784 | 802.429 | -13.6291 | 802.429 | -71.2301 | 802.429 | -126.841 |  | 802.429 | -43.2436 |
| 802.212 | 25.32438 | 803.267 | 15.75791 | 803.146 | 8.11827 | 803.146 | 8.54873 | 803.146 | -12.1002 | 803.146 | -68.2589 | 803.146 | -125.061 |  | 803.146 | -40.537 |
| 802.929 | 25.49144 | 803.982 | 14.98155 | 803.863 | 9.25793 | 803.863 | 9.12773 | 803.863 | -10.2105 | 803.863 | -67.1997 | 803.863 | -122.92 |  | 803.863 | -38.8161 |
| 803.646 | 25.65812 | 804.699 | 14.60045 | 804.579 | 10.54058 | 804.579 | 11.00241 | 804.579 | -8.30287 | 804.579 | -64.8454 | 804.579 | -120.761 |  | 804.579 | -36.953 |
| 804.364 | 25.82453 | 805.415 | 15.26618 | 805.296 | 12.21971 | 805.296 | 11.46023 | 805.296 | -7.46637 | 805.296 | -63.9073 | 805.296 | -119.673 |  | 805.296 | -34.6927 |
| 805.08 | 25.99072 | 806.132 | 16.15282 | 806.013 | 13.81102 | 806.013 | 14.45914 | 806.013 | -5.15241 | 806.013 | -60.4282 | 806.013 | -117.108 |  | 806.013 | -32.5201 |
| 805.798 | 26.15686 | 806.847 | 16.05773 | 806.729 | 15.60886 | 806.729 | 16.22862 | 806.729 | -2.48731 | 806.729 | -58.1791 | 806.729 | -114.192 |  | 806.729 | -30.1418 |
| 806.515 | 26.32309 | 807.563 | 16.30127 | 807.445 | 18.42123 | 807.445 | 18.71837 | 807.445 | 2.39636 | 807.445 | -55.2098 | 807.445 | -109.057 |  | 807.445 | -26.749 |
| 807.233 | 26.48973 | 808.28 | 17.68036 | 808.162 | 19.9334 | 808.162 | 20.23635 | 808.162 | 3.44454 | 808.162 | -53.2116 | 808.162 | -107.758 |  | 808.162 | -24.6556 |
| 807.949 | 26.65647 | 808.995 | 14.83345 | 808.878 | 22.98837 | 808.878 | 23.15431 | 808.878 | 5.5566 | 808.878 | -49.814 | 808.878 | -105.395 |  | 808.878 | -21.0202 |
| 808.665 | 26.82345 | 809.711 | 12.97245 | 809.594 | 25.73061 | 809.594 | 24.61627 | 809.594 | 8.7792 | 809.594 | -47.8725 | 809.594 | -101.921 |  | 809.594 | -17.6975 |
| 809.383 | 26.99057 | 810.427 | 14.339 | 810.31 | 29.17603 | 810.31 | 27.69757 | 810.31 | 12.41048 | 810.31 | -44.3116 | 810.31 | -98.0387 |  | 810.31 | -13.6716 |
| 810.099 | 27.15777 | 811.143 | 13.77245 | 811.026 | 31.4952 | 811.026 | 28.79759 | 811.026 | 16.40666 | 811.026 | -42.732 | 811.026 | -93.7915 |  | 811.026 | -10.772 |
| 810.817 | 27.32496 | 811.858 | 14.77709 | 811.742 | 33.94558 | 811.742 | 30.72399 | 811.742 | 18.62657 | 811.742 | -40.326 | 811.742 | -91.3206 |  | 811.742 | -7.74121 |
| 811.533 | 27.49187 | 812.574 | 16.29827 | 812.458 | 37.31795 | 812.458 | 33.25617 | 812.458 | 20.87393 | 812.458 | -37.3143 | 812.458 | -88.8222 |  | 812.458 | -3.78841 |
| 812.249 | 27.65818 | 813.29 | 15.79418 | 813.174 | 38.70936 | 813.174 | 36.08532 | 813.174 | 23.90286 | 813.174 | -34.0055 | 813.174 | -85.5423 |  | 813.174 | -1.81655 |
| 812.966 | 27.82365 | 814.004 | 17.53545 | 813.89 | 41.03845 | 813.89 | 37.47101 | 813.89 | 26.93586 | 813.89 | -32.1403 | 813.89 | -82.2583 |  | 813.89 | 1.09297 |
| 813.682 | 27.98799 | 814.72 | 18.04409 | 814.606 | 43.02128 | 814.606 | 38.94346 | 814.606 | 29.98886 | 814.606 | -30.1882 | 814.606 | -78.9543 |  | 814.606 | 3.65625 |
| 814.399 | 28.15079 | 815.435 | 19.14055 | 815.322 | 45.68827 | 815.322 | 42.22954 | 815.322 | 32.47617 | 815.322 | -26.4226 | 815.322 | -76.216 |  | 815.322 | 6.90367 |
| 815.115 | 28.31166 | 816.15 | 19.56709 | 816.036 | 48.1318 | 816.036 | 45.5349 | 816.036 | 36.23145 | 816.036 | -22.6389 | 816.036 | -72.2104 |  | 816.036 | 9.92602 |
| 815.83 | 28.47038 | 816.865 | 20.73536 | 816.751 | 51.47789 | 816.751 | 48.32166 | 816.751 | 39.14421 | 816.751 | -19.3733 | 816.751 | -69.047 |  | 816.751 | 13.85174 |
| 816.547 | 28.62665 | 817.581 | 21.62564 | 817.467 | 54.01633 | 817.467 | 49.71448 | 817.467 | 43.18109 | 817.467 | -17.5009 | 817.467 | -64.7592 |  | 817.467 | 16.97062 |
| 817.263 | 28.77982 | 818.295 | 19.06655 | 818.182 | 56.12599 | 818.182 | 52.66315 | 818.182 | 46.03376 | 818.182 | -14.0733 | 818.182 | -61.6558 |  | 818.182 | 19.6599 |
| 817.979 | 28.92958 | 819.01 | 19.69773 | 818.898 | 57.59232 | 818.898 | 54.6248 | 818.898 | 49.04515 | 818.898 | -11.6321 | 818.898 | -58.3935 |  | 818.898 | 21.70668 |
| 818.695 | 29.07569 | 819.724 | 19.382 | 819.613 | 59.67734 | 819.613 | 56.68114 | 819.613 | 53.99788 | 819.613 | -9.09681 | 819.613 | -53.1901 |  | 819.613 | 24.37133 |
| 819.41 | 29.21777 | 820.439 | 18.54936 | 820.328 | 62.38043 | 820.328 | 59.56817 | 820.328 | 58.25864 | 820.328 | -5.73087 | 820.328 | -48.6787 |  | 820.328 | 27.65404 |
| 820.127 | 29.35539 | 821.154 | 18.11218 | 821.043 | 65.61313 | 821.043 | 60.72463 | 821.043 | 61.29945 | 821.043 | -4.09549 | 821.043 | -45.3872 |  | 821.043 | 31.46637 |
| 820.842 | 29.48842 | 821.868 | 16.24582 | 821.758 | 69.17194 | 821.758 | 62.59649 | 821.758 | 63.47929 | 821.758 | -1.74473 | 821.758 | -42.9567 |  | 821.758 | 35.60481 |
| 821.557 | 29.61651 | 822.583 | 16.27873 | 822.473 | 71.04608 | 822.473 | 64.86023 | 822.473 | 67.56682 | 822.473 | 0.99793 | 822.473 | -38.6186 |  | 822.473 | 38.05858 |
| 822.273 | 29.73955 | 823.298 | 16.76255 | 823.187 | 73.52654 | 823.187 | 68.06864 | 823.187 | 71.24583 | 823.187 | 4.68458 | 823.187 | -34.6893 |  | 823.187 | 41.11786 |
| 822.988 | 29.85761 | 824.011 | 16.88945 | 823.902 | 75.77151 | 823.902 | 70.75413 | 823.902 | 75.65802 | 823.902 | 7.84898 | 823.902 | -30.0264 |  | 823.902 | 43.94246 |
| 823.703 | 29.97064 | 824.726 | 17.20164 | 824.616 | 77.29791 | 824.616 | 73.85215 | 824.616 | 79.98468 | 824.616 | 11.42524 | 824.616 | -25.4495 |  | 824.616 | 46.04768 |
| 824.419 | 30.07843 | 825.441 | 16.73591 | 825.331 | 79.47705 | 825.331 | 76.65526 | 825.331 | 82.08055 | 825.331 | 14.70727 | 825.331 | -23.1029 |  | 825.331 | 48.80645 |
| 825.134 | 30.18099 | 826.154 | 18.35973 | 826.046 | 81.7821 | 826.046 | 79.34258 | 826.046 | 84.91799 | 826.046 | 17.8735 | 826.046 | -20.0149 |  | 826.046 | 51.69113 |
| 825.849 | 30.27833 | 826.868 | 17.25191 | 826.76 | 84.56446 | 826.76 | 81.70068 | 826.76 | 89.26206 | 826.76 | 20.70984 | 826.76 | -15.4205 |  | 826.76 | 55.05231 |
| 826.565 | 30.37027 | 827.582 | 17.27055 | 827.475 | 87.5578 | 827.475 | 85.61641 | 827.475 | 92.21004 | 827.475 | 25.10449 | 827.475 | -12.2219 |  | 827.475 | 58.62527 |
| 827.279 | 30.45651 | 828.296 | 17.16691 | 828.188 | 89.8724 | 828.188 | 87.12261 | 828.188 | 97.31813 | 828.188 | 27.08825 | 828.188 | -6.86382 |  | 828.188 | 61.51788 |
| 827.993 | 30.53674 | 829.01 | 17.45345 | 828.902 | 92.37464 | 828.902 | 89.32646 | 828.902 | 101.5143 | 828.902 | 29.77035 | 828.902 | -2.41735 |  | 828.902 | 64.59894 |
| 828.709 | 30.61062 | 829.723 | 17.67073 | 829.617 | 93.58022 | 829.617 | 92.00053 | 829.617 | 105.7374 | 829.617 | 32.92334 | 829.617 | 2.05638 |  | 829.617 | 66.38415 |
| 829.424 | 30.67777 | 830.437 | 17.75745 | 830.331 | 94.9582 | 830.331 | 93.42986 | 830.331 | 108.3692 | 830.331 | 34.8309 | 830.331 | 4.93849 |  | 830.331 | 68.34095 |
| 830.138 | 30.73803 | 831.15 | 16.45155 | 831.045 | 97.00307 | 831.045 | 95.69006 | 831.045 | 112.0006 | 831.045 | 37.56935 | 831.045 | 8.82021 |  | 831.045 | 70.96464 |
| 830.853 | 30.7912 | 831.864 | 15.503 | 831.759 | 97.4564 | 831.759 | 98.10035 | 831.759 | 116.8246 | 831.759 | 40.45788 | 831.759 | 13.89443 |  | 831.759 | 71.99678 |
| 831.568 | 30.83716 | 832.578 | 16.13664 | 832.473 | 99.72251 | 832.473 | 100.0986 | 832.473 | 121.1013 | 832.473 | 42.93437 | 832.473 | 18.42145 |  | 832.473 | 74.84171 |
| 832.282 | 30.8756 | 833.291 | 16.18718 | 833.186 | 101.594 | 833.186 | 101.6927 | 833.186 | 124.4107 | 833.186 | 45.00605 | 833.186 | 21.98082 |  | 833.186 | 77.29117 |
| 832.997 | 30.90681 | 834.005 | 15.70209 | 833.9 | 104.2758 | 833.9 | 103.8204 | 833.9 | 125.9292 | 833.9 | 47.61196 | 833.9 | 23.74961 |  | 833.9 | 80.55184 |
| 833.711 | 30.93106 | 834.717 | 16.07427 | 834.613 | 105.5554 | 834.613 | 104.6505 | 834.613 | 129.4253 | 834.613 | 48.9197 | 834.613 | 27.4956 |  | 834.613 | 82.40939 |
| 834.425 | 30.94829 | 835.431 | 15.79045 | 835.327 | 108.4874 | 835.327 | 105.438 | 835.327 | 133.5315 | 835.327 | 50.18536 | 835.327 | 31.85214 |  | 835.327 | 85.9203 |
| 835.14 | 30.95849 | 836.143 | 16.58873 | 836.041 | 110.7096 | 836.041 | 107.2778 | 836.041 | 137.6001 | 836.041 | 52.50347 | 836.041 | 36.17102 |  | 836.041 | 88.72123 |
| 835.854 | 30.9615 | 836.857 | 16.44309 | 836.753 | 112.0008 | 836.753 | 109.9932 | 836.753 | 139.6821 | 836.753 | 55.69578 | 836.753 | 38.50261 |  | 836.753 | 90.58964 |
| 836.567 | 30.95884 | 837.571 | 16.69445 | 837.467 | 114.9979 | 837.467 | 112.5888 | 837.467 | 141.3627 | 837.467 | 58.7696 | 837.467 | 40.43351 |  | 837.467 | 94.16554 |
| 837.281 | 30.95078 | 838.283 | 16.41227 | 838.18 | 116.6244 | 838.18 | 113.9342 | 838.18 | 146.2314 | 838.18 | 60.59252 | 838.18 | 45.5522 |  | 838.18 | 96.37009 |
| 837.996 | 30.93774 | 838.996 | 16.88118 | 838.894 | 117.6537 | 838.894 | 116.5328 | 838.894 | 149.1308 | 838.894 | 63.66943 | 838.894 | 48.70183 |  | 838.894 | 97.9782 |
| 838.709 | 30.91963 | 839.708 | 18.41518 | 839.607 | 120.1456 | 839.607 | 116.4499 | 839.607 | 151.4922 | 839.607 | 64.06409 | 839.607 | 51.31322 |  | 839.607 | 101.0481 |
| 839.422 | 30.89666 | 840.421 | 18.85955 | 840.319 | 122.2652 | 840.319 | 117.6603 | 840.319 | 154.2842 | 840.319 | 65.7514 | 840.319 | 54.35481 |  | 840.319 | 103.7449 |
| 840.137 | 30.86895 | 841.133 | 19.30236 | 841.032 | 123.2252 | 841.032 | 118.2529 | 841.032 | 156.3111 | 841.032 | 66.82155 | 841.032 | 56.6317 |  | 841.032 | 105.2829 |
| 840.85 | 30.8367 | 841.846 | 20.75664 | 841.745 | 123.3726 | 841.745 | 119.6547 | 841.745 | 158.3717 | 841.745 | 68.70097 | 841.745 | 58.94221 |  | 841.745 | 106.0083 |
| 841.563 | 30.80031 | 842.558 | 20.89445 | 842.458 | 125.6354 | 842.458 | 120.741 | 842.458 | 159.2212 | 842.458 | 70.26482 | 842.458 | 60.0416 |  | 842.458 | 108.8491 |
| 842.277 | 30.76012 | 843.271 | 20.93755 | 843.171 | 126.9323 | 843.171 | 120.9858 | 843.171 | 160.2192 | 843.171 | 70.98718 | 843.171 | 61.28957 |  | 843.171 | 110.724 |
| 842.991 | 30.71658 | 843.983 | 20.68764 | 843.883 | 127.2718 | 843.883 | 120.1339 | 843.883 | 159.878 | 843.883 | 70.61219 | 843.883 | 61.19793 |  | 843.883 | 111.6408 |
| 843.704 | 30.67006 | 844.695 | 21.26936 | 844.596 | 128.2739 | 844.596 | 120.7603 | 844.596 | 162.4684 | 844.596 | 71.71614 | 844.596 | 64.0383 |  | 844.596 | 113.2209 |
| 844.417 | 30.62107 | 845.407 | 21.08609 | 845.309 | 129.3931 | 845.309 | 120.3254 | 845.309 | 163.398 | 845.309 | 71.7588 | 845.309 | 65.21784 |  | 845.309 | 114.918 |
| 845.13 | 30.56973 | 846.12 | 22.25145 | 846.021 | 129.9697 | 846.021 | 121.2444 | 846.021 | 163.3438 | 846.021 | 73.15469 | 846.021 | 65.41327 |  | 846.021 | 116.0719 |
| 845.844 | 30.51636 | 846.831 | 21.92045 | 846.733 | 129.7837 | 846.733 | 120.522 | 846.733 | 162.2974 | 846.733 | 72.90926 | 846.733 | 64.61644 |  | 846.733 | 116.463 |
| 846.556 | 30.46115 | 847.543 | 21.43373 | 847.445 | 129.7604 | 847.445 | 120.9531 | 847.445 | 161.5466 | 847.445 | 73.81726 | 847.445 | 64.11529 |  | 847.445 | 117.0169 |
| 847.269 | 30.40449 | 848.255 | 20.61745 | 848.158 | 128.7922 | 848.158 | 119.3593 | 848.158 | 162.6742 | 848.158 | 72.70104 | 848.158 | 65.49278 |  | 848.158 | 116.6268 |
| 847.982 | 30.34663 | 848.967 | 20.51709 | 848.87 | 127.8437 | 848.87 | 118.3897 | 848.87 | 162.5707 | 848.87 | 72.20826 | 848.87 | 65.6389 |  | 848.87 | 116.2554 |
| 848.695 | 30.28748 | 849.678 | 19.37373 | 849.583 | 127.0273 | 849.583 | 116.7969 | 849.583 | 162.1728 | 849.583 | 71.09303 | 849.583 | 65.49089 |  | 849.583 | 116.0171 |
| 849.408 | 30.22718 | 850.39 | 18.63091 | 850.294 | 126.2779 | 850.294 | 116.681 | 850.294 | 162.13 | 850.294 | 71.45338 | 850.294 | 65.6974 |  | 850.294 | 115.844 |
| 850.12 | 30.1658 | 851.101 | 18.76182 | 851.006 | 125.7402 | 851.006 | 116.3486 | 851.006 | 161.0041 | 851.006 | 71.59793 | 851.006 | 64.82112 |  | 851.006 | 115.8836 |
| 850.833 | 30.10359 | 851.814 | 18.53982 | 851.718 | 124.7689 | 851.718 | 114.3738 | 851.718 | 160.0165 | 851.718 | 70.10003 | 851.718 | 64.08307 |  | 851.718 | 115.4894 |
| 851.546 | 30.04082 | 852.524 | 17.69582 | 852.429 | 123.3087 | 852.429 | 112.047 | 852.429 | 160.0703 | 852.429 | 68.24946 | 852.429 | 64.38616 |  | 852.429 | 114.6056 |
| 852.258 | 29.97748 | 853.236 | 17.45555 | 853.141 | 122.3582 | 853.141 | 111.6812 | 853.141 | 159.6846 | 853.141 | 68.36055 | 853.141 | 64.25002 |  | 853.141 | 114.2323 |
| 852.97 | 29.91382 | 853.947 | 16.92964 | 853.853 | 121.284 | 853.853 | 111.152 | 853.853 | 156.7177 | 853.853 | 68.30822 | 853.853 | 61.53272 |  | 853.853 | 113.7353 |
| 853.682 | 29.85002 | 854.659 | 15.91927 | 854.565 | 119.5239 | 854.565 | 109.2024 | 854.565 | 156.2269 | 854.565 | 66.83559 | 854.565 | 61.29149 |  | 854.565 | 112.5524 |
| 854.394 | 29.78611 | 855.369 | 14.74418 | 855.275 | 118.1574 | 855.275 | 108.6022 | 855.275 | 154.7273 | 855.275 | 66.71088 | 855.275 | 60.0408 |  | 855.275 | 111.7615 |
| 855.108 | 29.72234 | 856.081 | 14.60545 | 855.987 | 116.2305 | 855.987 | 106.7989 | 855.987 | 153.1425 | 855.987 | 65.3845 | 855.987 | 58.7056 |  | 855.987 | 110.4118 |
| 855.819 | 29.65891 | 856.792 | 14.35518 | 856.699 | 115.0096 | 856.699 | 106.1547 | 856.699 | 149.3949 | 856.699 | 65.21721 | 856.699 | 55.20761 |  | 856.699 | 109.768 |
| 856.531 | 29.59609 | 857.503 | 15.01855 | 857.41 | 113.3471 | 857.41 | 105.1101 | 857.41 | 147.9732 | 857.41 | 64.64888 | 857.41 | 54.03516 |  | 857.41 | 108.6819 |
| 857.243 | 29.53375 | 858.213 | 15.79336 | 858.121 | 110.666 | 858.121 | 103.8499 | 858.121 | 146.5782 | 858.121 | 63.86493 | 858.121 | 52.88933 |  | 858.121 | 106.5772 |
| 857.954 | 29.47207 | 858.925 | 15.89082 | 858.832 | 108.9061 | 858.832 | 101.6828 | 858.832 | 144.6044 | 858.832 | 62.17399 | 858.832 | 51.16483 |  | 858.832 | 105.3937 |
| 858.667 | 29.41099 | 859.635 | 14.73027 | 859.544 | 107.0948 | 859.544 | 99.12249 | 859.544 | 142.3425 | 859.544 | 60.09061 | 859.544 | 49.15248 |  | 859.544 | 104.1596 |
| 859.379 | 29.35063 | 860.346 | 12.71782 | 860.254 | 104.6134 | 860.254 | 97.44579 | 860.254 | 139.8587 | 860.254 | 58.88948 | 860.254 | 46.91759 |  | 860.254 | 102.2538 |
| 860.09 | 29.29099 | 861.056 | 12.45709 | 860.965 | 103.1271 | 860.965 | 95.32284 | 860.965 | 137.0112 | 860.965 | 57.24277 | 860.965 | 44.31936 |  | 860.965 | 101.3439 |
| 860.802 | 29.23213 | 861.766 | 11.33682 | 861.676 | 101.2001 | 861.676 | 92.69941 | 861.676 | 134.2002 | 861.676 | 55.09556 | 861.676 | 41.7576 |  | 861.676 | 99.99328 |
| 861.513 | 29.17401 | 862.477 | 12.20136 | 862.386 | 98.72211 | 862.386 | 89.91257 | 862.386 | 131.7224 | 862.386 | 52.78429 | 862.386 | 39.52869 |  | 862.386 | 98.09088 |
| 862.224 | 29.11689 | 863.187 | 12.85864 | 863.097 | 97.09041 | 863.097 | 88.36107 | 863.097 | 128.9002 | 863.097 | 51.70902 | 863.097 | 36.95571 |  | 863.097 | 97.03557 |
| 862.936 | 29.06101 | 863.898 | 11.46164 | 863.808 | 94.55326 | 863.808 | 85.23398 | 863.808 | 124.6523 | 863.808 | 49.05816 | 863.808 | 32.95705 |  | 863.808 | 95.0748 |
| 863.648 | 29.00657 | 864.608 | 10.59873 | 864.519 | 92.16025 | 864.519 | 82.11542 | 864.519 | 121.0444 | 864.519 | 46.41584 | 864.519 | 29.59839 |  | 864.519 | 93.25817 |
| 864.359 | 28.95367 | 865.319 | 9.92255 | 865.229 | 89.40454 | 865.229 | 78.25918 | 865.229 | 116.1721 | 865.229 | 43.03516 | 865.229 | 24.97497 |  | 865.229 | 91.07804 |
| 865.069 | 28.90212 | 866.028 | 9.59509 | 865.94 | 86.57549 | 865.94 | 75.63074 | 865.94 | 110.5578 | 865.94 | 40.88296 | 865.94 | 19.60989 |  | 865.94 | 88.82538 |
| 865.78 | 28.85211 | 866.738 | 8.82091 | 866.65 | 83.60768 | 866.65 | 73.12921 | 866.65 | 106.5464 | 866.65 | 38.85698 | 866.65 | 15.84746 |  | 866.65 | 86.43315 |
| 866.491 | 28.80357 | 867.448 | 8.84691 | 867.36 | 80.9546 | 867.36 | 70.26519 | 867.36 | 102.62 | 867.36 | 36.46853 | 867.36 | 12.16988 |  | 867.36 | 84.35564 |
| 867.203 | 28.75657 | 868.157 | 10.45455 | 868.07 | 79.07548 | 868.07 | 67.26307 | 868.07 | 96.66196 | 868.07 | 33.94197 | 868.07 | 6.46078 |  | 868.07 | 83.0521 |
| 867.914 | 28.71076 | 868.868 | 10.05364 | 868.781 | 75.75145 | 868.781 | 63.06346 | 868.781 | 90.77136 | 868.781 | 30.2186 | 868.781 | 0.81943 |  | 868.781 | 80.30445 |
| 868.624 | 28.66577 | 869.577 | 9.33173 | 869.49 | 72.07377 | 869.49 | 60.52983 | 869.49 | 85.83623 | 869.49 | 28.15986 | 869.49 | -3.86716 |  | 869.49 | 77.20154 |
| 869.335 | 28.62139 | 870.286 | 8.02727 | 870.201 | 68.76431 | 870.201 | 57.74081 | 870.201 | 81.61681 | 870.201 | 25.84707 | 870.201 | -7.83733 |  | 870.201 | 74.46846 |
| 870.045 | 28.5778 | 870.997 | 6.27873 | 870.91 | 65.75569 | 870.91 | 55.92593 | 870.91 | 76.96839 | 870.91 | 24.50708 | 870.91 | -12.2372 |  | 870.91 | 72.0346 |
| 870.756 | 28.53517 | 871.706 | 5.77418 | 871.62 | 61.38316 | 871.62 | 53.23422 | 871.62 | 72.073 | 871.62 | 22.29094 | 871.62 | -16.8837 |  | 871.62 | 68.23765 |
| 871.466 | 28.49339 | 872.416 | 5.91664 | 872.33 | 58.14105 | 872.33 | 50.61869 | 872.33 | 67.67115 | 872.33 | 20.15097 | 872.33 | -21.0367 |  | 872.33 | 65.57112 |
| 872.176 | 28.45241 | 873.125 | 5.52227 | 873.039 | 55.36723 | 873.039 | 44.9008 | 873.039 | 62.10435 | 873.039 | 14.90797 | 873.039 | -26.3549 |  | 873.039 | 63.37206 |
| 872.888 | 28.41188 | 873.833 | 3.97373 | 873.749 | 51.5536 | 873.749 | 41.58562 | 873.749 | 59.42769 | 873.749 | 12.06835 | 873.749 | -28.7827 |  | 873.749 | 60.13401 |
| 873.598 | 28.37166 | 874.543 | 3.92918 | 874.459 | 48.03686 | 874.459 | 38.79056 | 874.459 | 54.07226 | 874.459 | 9.74886 | 874.459 | -33.8892 |  | 874.459 | 57.19285 |
| 874.308 | 28.33156 | 875.252 | 4.98018 | 875.168 | 46.02077 | 875.168 | 36.40587 | 875.168 | 50.38993 | 875.168 | 7.83907 | 875.168 | -37.323 |  | 875.168 | 55.75152 |
| 875.018 | 28.29153 | 875.96 | 5.27882 | 875.878 | 43.03625 | 875.878 | 33.96944 | 875.878 | 46.42882 | 875.878 | 5.8782 | 875.878 | -41.0352 |  | 875.878 | 53.34257 |
| 875.728 | 28.25108 | 876.67 | 5.40709 | 876.587 | 39.80295 | 876.587 | 31.0318 | 876.587 | 41.80742 | 876.587 | 3.41545 | 876.587 | -45.4081 |  | 876.587 | 50.68404 |
| 876.438 | 28.21033 | 877.379 | 5.97864 | 877.296 | 37.2191 | 877.296 | 28.90091 | 877.296 | 38.76641 | 877.296 | 1.75946 | 877.296 | -48.2006 |  | 877.296 | 48.67495 |
| 877.148 | 28.16882 | 878.088 | 7.26645 | 878.005 | 35.20543 | 878.005 | 28.11778 | 878.005 | 35.55403 | 878.005 | 1.45122 | 878.005 | -51.1644 |  | 878.005 | 47.23605 |
| 877.857 | 28.12632 | 878.797 | 7.425 | 878.714 | 30.82568 | 878.714 | 24.23606 | 878.714 | 32.96724 | 878.714 | -1.95561 | 878.714 | -53.5026 |  | 878.714 | 43.43106 |
| 878.567 | 28.08281 | 879.505 | 8.18955 | 879.423 | 28.6695 | 879.423 | 22.23291 | 879.423 | 29.37011 | 879.423 | -3.48387 | 879.423 | -56.8512 |  | 879.423 | 41.84965 |
| 879.278 | 28.03812 | 880.214 | 6.92682 | 880.133 | 26.03093 | 880.133 | 21.0017 | 880.133 | 28.73553 | 880.133 | -4.23951 | 880.133 | -57.2369 |  | 880.133 | 39.78665 |
| 879.987 | 27.99205 | 880.922 | 5.71164 | 880.841 | 24.04968 | 880.841 | 18.61975 | 880.841 | 25.21103 | 880.841 | -6.14724 | 880.841 | -60.5132 |  | 880.841 | 38.37936 |
| 880.697 | 27.94427 | 881.63 | 6.79227 | 881.55 | 21.76843 | 881.55 | 16.89919 | 881.55 | 23.08679 | 881.55 | -7.3929 | 881.55 | -62.3889 |  | 881.55 | 36.67287 |
| 881.406 | 27.89462 | 882.34 | 5.85291 | 882.258 | 19.09016 | 882.258 | 15.27618 | 882.258 | 21.01196 | 882.258 | -8.54169 | 882.258 | -64.2156 |  | 882.258 | 34.56856 |
| 882.115 | 27.84292 | 883.047 | 5.11109 | 882.967 | 16.98267 | 882.967 | 12.59683 | 882.967 | 19.7815 | 882.967 | -10.7462 | 882.967 | -65.1975 |  | 882.967 | 33.03583 |
| 882.825 | 27.78895 | 883.755 | 3.76427 | 883.677 | 15.79049 | 883.677 | 11.27702 | 883.677 | 17.73487 | 883.677 | -11.5904 | 883.677 | -66.9952 |  | 883.677 | 32.41923 |
| 883.534 | 27.73282 | 884.464 | 3.21164 | 884.384 | 14.4821 | 884.384 | 10.17411 | 884.384 | 13.93394 | 884.384 | -12.2198 | 884.384 | -70.5483 |  | 884.384 | 31.68398 |
| 884.243 | 27.6746 | 885.172 | 3.24945 | 885.093 | 12.18351 | 885.093 | 8.3587 | 885.093 | 10.69393 | 885.093 | -13.5603 | 885.093 | -73.5398 |  | 885.093 | 29.96016 |
| 884.952 | 27.61404 | 885.88 | 2.99291 | 885.801 | 10.87848 | 885.801 | 6.7412 | 885.801 | 8.54465 | 885.801 | -14.7035 | 885.801 | -75.4409 |  | 885.801 | 29.22908 |
| 885.661 | 27.5512 | 886.589 | 2.598 | 886.51 | 9.06818 | 886.51 | 7.13815 | 886.51 | 7.51212 | 886.51 | -13.8317 | 886.51 | -76.2248 |  | 886.51 | 27.99354 |
| 886.37 | 27.4858 | 887.296 | 1.66091 | 887.217 | 7.33186 | 887.217 | 5.90626 | 887.217 | 7.20424 | 887.217 | -14.59 | 887.217 | -76.2849 |  | 887.217 | 26.83037 |
| 887.079 | 27.41753 | 888.003 | 1.51309 | 887.926 | 6.35789 | 887.926 | 5.38655 | 887.926 | 6.26233 | 887.926 | -14.6349 | 887.926 | -76.9783 |  | 887.926 | 26.43116 |
| 887.787 | 27.34626 | 888.711 | 2.16709 | 888.635 | 6.17922 | 888.635 | 4.87686 | 888.635 | 3.7481 | 888.635 | -14.6697 | 888.635 | -79.2439 |  | 888.635 | 26.82726 |
| 888.496 | 27.27208 | 889.419 | 1.78336 | 889.342 | 4.31518 | 889.342 | 3.21716 | 889.342 | 2.55092 | 889.342 | -15.8558 | 889.342 | -80.1933 |  | 889.342 | 25.53636 |
| 889.205 | 27.19488 | 890.126 | 3.366 | 890.05 | 2.18527 | 890.05 | 2.11601 | 890.05 | 2.83932 | 890.05 | -16.4827 | 890.05 | -79.6567 |  | 890.05 | 23.98041 |
| 889.915 | 27.11498 | 890.834 | 2.83918 | 890.758 | 2.37635 | 890.758 | 0.90133 | 890.758 | 1.18869 | 890.758 | -17.2232 | 890.758 | -81.0591 |  | 890.758 | 24.74544 |
| 890.623 | 27.03266 | 891.542 | 3.08418 | 891.466 | 1.7624 | 891.466 | 0.68471 | 891.466 | 0.63244 | 891.466 | -16.9656 | 891.466 | -81.3672 |  | 891.466 | 24.70545 |
| 891.332 | 26.94845 | 892.249 | 3.88718 | 892.173 | 1.05378 | 892.173 | 0.81502 | 892.173 | -1.01818 | 892.173 | -16.3617 | 892.173 | -82.77 |  | 892.173 | 24.56997 |
| 892.04 | 26.86254 | 892.956 | 4.17127 | 892.881 | -1.0559 | 892.881 | -1.08215 | 892.881 | 0.64529 | 892.881 | -17.7847 | 892.881 | -80.8583 |  | 892.881 | 23.32476 |
| 892.748 | 26.77548 | 893.664 | 3.44655 | 893.588 | -1.69472 | 893.588 | -0.0318 | 893.588 | 0.06224 | 893.588 | -16.2608 | 893.588 | -81.1935 |  | 893.588 | 23.9486 |
| 893.457 | 26.68757 | 894.371 | 4.191 | 894.296 | -2.27705 | 894.296 | -0.93024 | 894.296 | -1.07466 | 894.296 | -15.6855 | 894.296 | -81.1432 |  | 894.296 | 24.63072 |
| 894.165 | 26.59867 | 895.078 | 4.884 | 895.003 | -3.1205 | 895.003 | -2.17063 | 895.003 | -2.43149 | 895.003 | -14.9961 | 895.003 | -80.884 |  | 895.003 | 25.04993 |
| 894.873 | 26.50923 | 895.784 | 5.55827 | 895.711 | -4.46823 | 895.711 | -3.87902 | 895.711 | -4.00111 | 895.711 | -14.7719 | 895.711 | -80.8353 |  | 895.711 | 24.96665 |
| 895.581 | 26.41954 | 896.492 | 4.72145 | 896.419 | -5.26612 | 896.419 | -5.01821 | 896.419 | -5.44112 | 896.419 | -13.9786 | 896.419 | -80.6571 |  | 896.419 | 25.43321 |
| 896.289 | 26.33002 | 897.199 | 4.46818 | 897.125 | -6.41214 | 897.125 | -6.74152 | 897.125 | -6.81139 | 897.125 | -13.7748 | 897.125 | -80.4136 |  | 897.125 | 25.54806 |
| 896.997 | 26.24082 | 897.905 | 2.64918 | 897.833 | -6.73677 | 897.833 | -7.40929 | 897.833 | -6.66967 | 897.833 | -12.5101 | 897.833 | -78.6536 |  | 897.833 | 26.48788 |
| 897.704 | 26.15217 | 898.612 | 2.81509 | 898.54 | -7.19565 | 898.54 | -8.33235 | 898.54 | -7.30523 | 898.54 | -11.5033 | 898.54 | -77.6732 |  | 898.54 | 27.29167 |
| 898.412 | 26.06436 | 899.319 | 3.15709 | 899.247 | -8.00114 | 899.247 | -9.10581 | 899.247 | -8.38507 | 899.247 | -10.347 | 899.247 | -77.137 |  | 899.247 | 27.74883 |
| 899.12 | 25.9776 | 900.025 | 2.66927 | 899.954 | -8.76147 | 899.954 | -10.274 | 899.954 | -7.9462 | 899.954 | -9.58534 | 899.954 | -75.0821 |  | 899.954 | 28.25116 |
| 899.828 | 25.89217 | 900.732 | 1.03227 | 900.661 | -8.79861 | 900.661 | -10.9386 | 900.661 | -7.18691 | 900.661 | -8.32016 | 900.661 | -72.7069 |  | 900.661 | 29.47669 |
| 900.535 | 25.80833 | 901.438 | 1.60282 | 901.367 | -9.31682 | 901.367 | -10.9326 | 901.367 | -6.53008 | 901.367 | -6.38709 | 901.367 | -70.4363 |  | 901.367 | 30.21936 |
| 901.243 | 25.72593 | 902.145 | 3.139 | 902.075 | -8.71228 | 902.075 | -10.7969 | 902.075 | -4.64758 | 902.075 | -4.3189 | 902.075 | -66.9355 |  | 902.075 | 32.08834 |
| 901.95 | 25.64496 | 902.851 | 4.15764 | 902.781 | -8.34432 | 902.781 | -10.9527 | 902.781 | -4.21013 | 902.781 | -2.5476 | 902.781 | -64.8844 |  | 902.781 | 33.71718 |
| 902.657 | 25.56579 | 903.557 | 4.79282 | 903.488 | -8.23534 | 903.488 | -11.1676 | 903.488 | -2.73371 | 903.488 | -0.83276 | 903.488 | -61.7919 |  | 903.488 | 35.08882 |
| 903.365 | 25.48872 | 904.263 | 4.957 | 904.194 | -8.3294 | 904.194 | -11.1838 | 904.194 | -1.17451 | 904.194 | 1.07819 | 904.194 | -58.619 |  | 904.194 | 36.25564 |
| 904.072 | 25.41417 | 904.97 | 5.59918 | 904.901 | -8.27338 | 904.901 | -9.70745 | 904.901 | 0.06138 | 904.901 | 4.48429 | 904.901 | -55.7671 |  | 904.901 | 37.57432 |
| 904.779 | 25.34226 | 905.676 | 7.25455 | 905.607 | -8.14575 | 905.607 | -9.80377 | 905.607 | 2.32633 | 905.607 | 6.31503 | 905.607 | -51.8885 |  | 905.607 | 38.96282 |
| 905.486 | 25.27311 | 906.381 | 7.49309 | 906.314 | -7.53688 | 906.314 | -10.8263 | 906.314 | 4.91346 | 906.314 | 7.2223 | 906.314 | -47.6853 |  | 906.314 | 40.83436 |
| 906.193 | 25.20675 | 907.087 | 7.52373 | 907.019 | -7.29262 | 907.019 | -10.9471 | 907.019 | 6.9372 | 907.019 | 9.02586 | 907.019 | -44.0502 |  | 907.019 | 42.33771 |
| 906.9 | 25.14365 | 907.792 | 8.37945 | 907.725 | -6.63927 | 907.725 | -11.2204 | 907.725 | 8.42871 | 907.725 | 10.67961 | 907.725 | -40.9449 |  | 907.725 | 44.25193 |
| 907.606 | 25.08381 | 908.499 | 9.23082 | 908.432 | -6.67861 | 908.432 | -11.3421 | 908.432 | 10.22628 | 908.432 | 12.48771 | 908.432 | -37.5314 |  | 908.432 | 45.47525 |
| 908.312 | 25.02726 | 909.205 | 8.42982 | 909.137 | -6.26727 | 909.137 | -8.4707 | 909.137 | 11.87766 | 909.137 | 17.28345 | 909.137 | -34.2686 |  | 909.137 | 47.14569 |
| 909.019 | 24.97444 | 909.91 | 6.10373 | 909.844 | -5.18802 | 909.844 | -8.91059 | 909.844 | 12.23642 | 909.844 | 18.77335 | 909.844 | -32.2938 |  | 909.844 | 49.48761 |
| 909.726 | 24.9254 | 910.615 | 5.102 | 910.549 | -3.58632 | 910.549 | -8.59035 | 910.549 | 14.06444 | 910.549 | 21.01794 | 910.549 | -28.8544 |  | 910.549 | 52.34839 |
| 910.432 | 24.88013 | 911.32 | 5.12491 | 911.255 | -3.45907 | 911.255 | -8.39516 | 911.255 | 14.89615 | 911.255 | 23.14019 | 911.255 | -26.4089 |  | 911.255 | 53.73652 |
| 911.139 | 24.83865 | 912.027 | 6.087 | 911.961 | -4.18152 | 911.961 | -7.73053 | 911.961 | 15.6931 | 911.961 | 25.73188 | 911.961 | -23.9983 |  | 911.961 | 54.27495 |
| 911.846 | 24.80107 | 912.732 | 6.53273 | 912.667 | -4.34156 | 912.667 | -7.03336 | 912.667 | 18.14557 | 912.667 | 28.35612 | 912.667 | -19.9321 |  | 912.667 | 55.37578 |
| 912.552 | 24.76716 | 913.437 | 5.96864 | 913.372 | -3.36265 | 913.372 | -7.23343 | 913.372 | 19.03378 | 913.372 | 30.08039 | 913.372 | -17.4325 |  | 913.372 | 57.61378 |
| 913.258 | 24.73699 | 914.142 | 6.78873 | 914.078 | -2.67307 | 914.078 | -8.90209 | 914.078 | 19.6859 | 914.078 | 30.3388 | 914.078 | -15.1666 |  | 914.078 | 59.56424 |
| 913.965 | 24.71033 | 914.847 | 6.20836 | 914.783 | -1.62805 | 914.783 | -7.77133 | 914.783 | 19.96374 | 914.783 | 33.3939 | 914.783 | -13.2774 |  | 914.783 | 61.86834 |
| 914.671 | 24.6871 | 915.551 | 5.13464 | 915.488 | -1.30472 | 915.488 | -6.90939 | 915.488 | 21.58794 | 915.488 | 36.18018 | 915.488 | -10.0417 |  | 915.488 | 63.45077 |
| 915.377 | 24.66723 | 916.257 | 5.38127 | 916.194 | 1.07168 | 916.194 | -6.41582 | 916.194 | 21.00611 | 916.194 | 38.60082 | 916.194 | -9.00985 |  | 916.194 | 67.08804 |
| 916.083 | 24.65059 | 916.962 | 5.81682 | 916.899 | 1.76599 | 916.899 | -5.68228 | 916.899 | 21.92593 | 916.899 | 41.25869 | 916.899 | -6.4786 |  | 916.899 | 69.04145 |
| 916.789 | 24.63701 | 917.667 | 7.41773 | 917.604 | 1.73317 | 917.604 | -5.00402 | 917.604 | 22.31703 | 917.604 | 43.86129 | 917.604 | -4.47606 |  | 917.604 | 70.26771 |
| 917.495 | 24.62637 | 918.371 | 7.188 | 918.309 | 3.84009 | 918.309 | -4.65326 | 918.309 | 24.0897 | 918.309 | 46.13639 | 918.309 | -1.09197 |  | 918.309 | 73.63373 |
| 918.199 | 24.61896 | 919.076 | 6.467 | 919.013 | 4.99494 | 919.013 | -2.51972 | 919.013 | 23.98126 | 919.013 | 50.19154 | 919.013 | 0.40874 |  | 919.013 | 76.04587 |
| 918.905 | 24.61488 | 919.78 | 6.15918 | 919.719 | 4.96789 | 919.719 | -1.62937 | 919.719 | 24.80719 | 919.719 | 53.00896 | 919.719 | 2.84838 |  | 919.719 | 77.2797 |
| 919.611 | 24.61419 | 920.486 | 4.34782 | 920.424 | 5.51532 | 920.424 | -0.2332 | 920.424 | 26.66304 | 920.424 | 56.32946 | 920.424 | 6.31565 |  | 920.424 | 79.08623 |
| 920.317 | 24.61691 | 921.19 | 3.52055 | 921.129 | 7.46634 | 921.129 | 1.27184 | 921.129 | 28.75766 | 921.129 | 59.75884 | 921.129 | 10.0217 |  | 921.129 | 82.29633 |
| 921.022 | 24.62304 | 921.894 | 1.73 | 921.833 | 9.1081 | 921.833 | 3.20269 | 921.833 | 29.75652 | 921.833 | 63.6113 | 921.833 | 12.6297 |  | 921.833 | 85.1954 |
| 921.728 | 24.63227 | 922.598 | 1.77427 | 922.537 | 10.30388 | 922.537 | 2.47696 | 922.537 | 30.59658 | 922.537 | 64.80718 | 922.537 | 15.07891 |  | 922.537 | 87.64848 |
| 922.433 | 24.64464 | 923.302 | 2.537 | 923.243 | 12.15283 | 923.243 | 2.98016 | 923.243 | 31.22642 | 923.243 | 67.23745 | 923.243 | 17.32246 |  | 923.243 | 90.75831 |
| 923.139 | 24.65986 | 924.006 | 3.34927 | 923.947 | 13.70763 | 923.947 | 3.91972 | 923.947 | 32.78172 | 923.947 | 70.09862 | 923.947 | 20.4869 |  | 923.947 | 93.57041 |
| 923.844 | 24.67789 | 924.71 | 3.27627 | 924.652 | 14.24097 | 924.652 | 3.55944 | 924.652 | 33.76923 | 924.652 | 71.66268 | 924.652 | 23.08584 |  | 924.652 | 95.36285 |
| 924.548 | 24.69859 | 925.414 | 1.97509 | 925.356 | 15.49521 | 925.356 | 3.95825 | 925.356 | 34.05553 | 925.356 | 73.98309 | 925.356 | 24.98128 |  | 925.356 | 97.87439 |
| 925.253 | 24.72192 | 926.119 | 2.64127 | 926.06 | 17.9195 | 926.06 | 5.82063 | 926.06 | 33.71472 | 926.06 | 77.76709 | 926.06 | 26.24962 |  | 926.06 | 101.556 |
| 925.958 | 24.74775 | 926.823 | 2.93618 | 926.765 | 18.35098 | 926.765 | 8.13985 | 926.765 | 33.84338 | 926.765 | 82.01064 | 926.765 | 27.98971 |  | 926.765 | 103.2466 |
| 926.663 | 24.7757 | 927.526 | 2.85045 | 927.468 | 18.79963 | 927.468 | 8.93421 | 927.468 | 34.84155 | 927.468 | 84.72388 | 927.468 | 30.59473 |  | 927.468 | 104.9507 |
| 927.368 | 24.80581 | 928.23 | 4.23436 | 928.173 | 18.26444 | 928.173 | 9.26008 | 928.173 | 35.5278 | 928.173 | 86.97409 | 928.173 | 32.8924 |  | 928.173 | 105.6746 |
| 928.073 | 24.83814 | 928.934 | 4.259 | 928.877 | 19.98818 | 928.877 | 10.11858 | 928.877 | 34.5793 | 928.877 | 89.75419 | 928.877 | 33.55305 |  | 928.877 | 108.6557 |
| 928.778 | 24.87216 | 929.637 | 4.79673 | 929.58 | 19.70264 | 929.58 | 9.2805 | 929.58 | 35.10614 | 929.58 | 90.835 | 929.58 | 35.68675 |  | 929.58 | 109.6256 |
| 929.483 | 24.90796 | 930.34 | 5.58036 | 930.285 | 20.38798 | 930.285 | 8.91004 | 930.285 | 34.13075 | 930.285 | 92.38888 | 930.285 | 36.32278 |  | 930.285 | 111.5701 |
| 930.186 | 24.94547 | 931.044 | 5.17318 | 930.988 | 21.09227 | 930.988 | 8.99199 | 930.988 | 33.25799 | 930.988 | 94.38971 | 930.988 | 37.05688 |  | 930.988 | 113.5299 |
| 930.891 | 24.98427 | 931.747 | 5.35355 | 931.692 | 21.41369 | 931.692 | 8.89071 | 931.692 | 32.5726 | 931.692 | 96.21003 | 931.692 | 37.98063 |  | 931.692 | 115.1086 |
| 931.596 | 25.0243 | 932.45 | 6.37927 | 932.396 | 21.71404 | 932.396 | 9.02679 | 932.396 | 32.21181 | 932.396 | 98.26772 | 932.396 | 39.22899 |  | 932.396 | 116.6663 |
| 932.3 | 25.06558 | 933.155 | 8.45855 | 933.099 | 22.00159 | 933.099 | 9.22944 | 933.099 | 32.00068 | 933.099 | 100.3893 | 933.099 | 40.62471 |  | 933.099 | 118.2093 |
| 933.005 | 25.1082 | 933.858 | 7.33155 | 933.802 | 21.56487 | 933.802 | 9.08842 | 933.802 | 31.69734 | 933.802 | 102.1671 | 933.802 | 41.92823 |  | 933.802 | 119.0281 |
| 933.709 | 25.1525 | 934.561 | 7.69691 | 934.507 | 21.53571 | 934.507 | 10.29404 | 934.507 | 32.57099 | 934.507 | 105.2971 | 934.507 | 44.4133 |  | 934.507 | 120.2581 |
| 934.412 | 25.19841 | 935.263 | 8.67009 | 935.21 | 21.01357 | 935.21 | 10.89131 | 935.21 | 31.41912 | 935.21 | 107.8132 | 935.21 | 44.86829 |  | 935.21 | 120.9914 |
| 935.116 | 25.24579 | 935.966 | 9.54018 | 935.912 | 20.80705 | 935.912 | 10.47475 | 935.912 | 30.88493 | 935.912 | 109.3128 | 935.912 | 45.93867 |  | 935.912 | 122.0387 |
| 935.821 | 25.29439 | 936.669 | 10.087 | 936.617 | 21.72209 | 936.617 | 10.70928 | 936.617 | 29.38345 | 936.617 | 111.4717 | 936.617 | 46.04862 |  | 936.617 | 124.2128 |
| 936.525 | 25.34416 | 937.372 | 10.24082 | 937.319 | 21.49787 | 937.319 | 10.56502 | 937.319 | 29.56396 | 937.319 | 113.2436 | 937.319 | 47.8337 |  | 937.319 | 125.2423 |
| 937.229 | 25.39526 | 938.074 | 8.93909 | 938.022 | 20.92181 | 938.022 | 9.56248 | 938.022 | 27.98981 | 938.022 | 114.1599 | 938.022 | 47.86641 |  | 938.022 | 125.9218 |
| 937.933 | 25.44722 | 938.777 | 8.64327 | 938.726 | 20.95839 | 938.726 | 10.74282 | 938.726 | 27.03016 | 938.726 | 117.2619 | 938.726 | 48.51589 |  | 938.726 | 127.2156 |
| 938.635 | 25.49981 | 939.48 | 7.13109 | 939.428 | 20.62764 | 939.428 | 11.67909 | 939.428 | 25.93333 | 939.428 | 120.1143 | 939.428 | 49.02364 |  | 939.428 | 128.1386 |
| 939.339 | 25.553 | 940.182 | 5.55609 | 940.131 | 20.515 | 940.131 | 10.94761 | 940.131 | 24.62191 | 940.131 | 121.3017 | 940.131 | 49.31907 |  | 940.131 | 129.2815 |
| 940.043 | 25.60694 | 940.884 | 4.392 | 940.835 | 20.96066 | 940.835 | 10.92448 | 940.835 | 24.49058 | 940.835 | 123.2001 | 940.835 | 50.79688 |  | 940.835 | 130.9845 |
| 940.747 | 25.66188 | 941.587 | 6.07845 | 941.537 | 20.74633 | 941.537 | 10.85775 | 941.537 | 23.75113 | 941.537 | 125.0496 | 941.537 | 51.66201 |  | 941.537 | 132.0239 |
| 941.451 | 25.71782 | 942.289 | 5.41791 | 942.239 | 20.41542 | 942.239 | 12.35091 | 942.239 | 23.48074 | 942.239 | 128.4589 | 942.239 | 52.99619 |  | 942.239 | 132.9467 |
| 942.153 | 25.77473 | 942.991 | 4.238 | 942.941 | 20.28264 | 942.941 | 12.76434 | 942.941 | 22.55195 | 942.941 | 130.7885 | 942.941 | 53.67197 |  | 942.941 | 134.0676 |
| 942.856 | 25.83267 | 943.693 | 2.764 | 943.645 | 20.36227 | 943.645 | 13.78734 | 943.645 | 21.57889 | 943.645 | 133.7331 | 943.645 | 54.30805 |  | 943.645 | 135.4046 |
| 943.56 | 25.89192 | 944.395 | 2.58064 | 944.347 | 20.67576 | 944.347 | 13.38744 | 944.347 | 19.75729 | 944.347 | 135.2493 | 944.347 | 54.09103 |  | 944.347 | 136.9718 |
| 944.263 | 25.95235 | 945.097 | 0.56255 | 945.049 | 20.52057 | 945.049 | 11.62494 | 945.049 | 19.22863 | 945.049 | 135.403 | 945.049 | 55.16693 |  | 945.049 | 138.0703 |
| 944.965 | 26.01379 | 945.799 | 1.10582 | 945.752 | 19.82996 | 945.752 | 11.56705 | 945.752 | 19.31574 | 945.752 | 137.264 | 945.752 | 56.8609 |  | 945.752 | 138.6352 |
| 945.669 | 26.07628 | 946.501 | 1.20536 | 946.454 | 18.81435 | 946.454 | 10.24511 | 946.454 | 18.45341 | 946.454 | 137.8582 | 946.454 | 57.60314 |  | 946.454 | 138.8734 |
| 946.372 | 26.13998 | 947.203 | 1.04464 | 947.156 | 18.16512 | 947.156 | 9.39288 | 947.156 | 18.6257 | 947.156 | 138.9221 | 947.156 | 59.38 |  | 947.156 | 139.4779 |
| 947.075 | 26.20487 | 947.905 | 1.75036 | 947.857 | 18.05346 | 947.857 | 9.46838 | 947.857 | 17.86853 | 947.857 | 140.911 | 947.857 | 60.22512 |  | 947.857 | 140.6182 |
| 947.778 | 26.27095 | 948.606 | 1.09936 | 948.56 | 18.5664 | 948.56 | 8.80737 | 948.56 | 14.83208 | 948.56 | 142.1689 | 948.56 | 58.79552 |  | 948.56 | 142.3866 |
| 948.48 | 26.33856 | 949.308 | -0.32582 | 949.262 | 17.43984 | 949.262 | 8.66761 | 949.262 | 13.63304 | 949.262 | 143.9453 | 949.262 | 59.20105 |  | 949.262 | 142.5138 |
| 949.183 | 26.40743 | 950.009 | -0.53373 | 949.964 | 17.11438 | 949.964 | 8.76169 | 949.964 | 13.9543 | 949.964 | 145.9555 | 949.964 | 61.12688 |  | 949.964 | 143.4421 |
| 949.885 | 26.47733 | 950.711 | -0.60182 | 950.665 | 17.64823 | 950.665 | 8.70584 | 950.665 | 13.45082 | 950.665 | 147.8131 | 950.665 | 62.22569 |  | 950.665 | 145.2279 |
| 950.588 | 26.54815 | 951.412 | -1.02382 | 951.368 | 17.81292 | 951.368 | 8.55186 | 951.368 | 12.40378 | 951.368 | 149.578 | 951.368 | 62.7855 |  | 951.368 | 146.6481 |
| 951.29 | 26.61973 | 952.113 | 0.28127 | 952.069 | 16.5707 | 952.069 | 8.21444 | 952.069 | 11.79769 | 952.069 | 151.154 | 952.069 | 63.7817 |  | 952.069 | 146.6578 |
| 951.992 | 26.69188 | 952.815 | 2.32991 | 952.77 | 16.29313 | 952.77 | 8.15775 | 952.77 | 11.76806 | 952.77 | 153.0107 | 952.77 | 65.35436 |  | 952.77 | 147.6322 |
| 952.695 | 26.7646 | 953.516 | 1.39973 | 953.471 | 16.14646 | 953.471 | 7.19195 | 953.471 | 9.49187 | 953.471 | 153.9583 | 953.471 | 64.68045 |  | 953.471 | 148.7374 |
| 953.397 | 26.83774 | 954.217 | 0.49064 | 954.174 | 15.05568 | 954.174 | 7.05251 | 954.174 | 8.07087 | 954.174 | 155.7378 | 954.174 | 64.8663 |  | 954.174 | 148.9022 |
| 954.099 | 26.91126 | 954.918 | -0.59418 | 954.875 | 13.85963 | 954.875 | 7.05909 | 954.875 | 8.4194 | 954.875 | 157.6578 | 954.875 | 66.81712 |  | 954.875 | 148.9581 |
| 954.801 | 26.9856 | 955.619 | -0.32855 | 955.576 | 13.2889 | 955.576 | 6.38118 | 955.576 | 8.04056 | 955.576 | 158.8933 | 955.576 | 68.04056 |  | 955.576 | 149.6393 |
| 955.503 | 27.06084 | 956.32 | 0.41664 | 956.277 | 12.94632 | 956.277 | 5.09339 | 956.277 | 7.26437 | 956.277 | 159.5189 | 956.277 | 68.86666 |  | 956.277 | 150.5487 |
| 956.204 | 27.13711 | 957.021 | 2.99327 | 956.979 | 12.5117 | 956.979 | 4.22713 | 956.979 | 5.37451 | 956.979 | 160.5688 | 956.979 | 68.58137 |  | 956.979 | 151.3678 |
| 956.906 | 27.21435 | 957.722 | 3.67864 | 957.68 | 11.15011 | 957.68 | 3.16914 | 957.68 | 5.25062 | 957.68 | 161.4242 | 957.68 | 70.05976 |  | 957.68 | 151.2581 |
| 957.609 | 27.29261 | 958.422 | 4.29255 | 958.381 | 10.03313 | 958.381 | 3.2295 | 958.381 | 3.73075 | 958.381 | 163.398 | 958.381 | 70.14218 |  | 958.381 | 151.3931 |
| 958.311 | 27.37176 | 959.123 | 5.11618 | 959.081 | 8.65122 | 959.081 | 3.31999 | 959.081 | 1.64649 | 959.081 | 165.3992 | 959.081 | 69.65792 |  | 959.081 | 151.2614 |
| 959.011 | 27.45167 | 959.824 | 2.71645 | 959.782 | 7.91016 | 959.782 | 3.21743 | 959.782 | -0.54414 | 959.782 | 167.21 | 959.782 | 69.06958 |  | 959.782 | 151.7722 |
| 959.713 | 27.53214 | 960.524 | 3.54082 | 960.484 | 7.10482 | 960.484 | 3.88318 | 960.484 | -1.48828 | 960.484 | 169.7919 | 960.484 | 69.73001 |  | 960.484 | 152.2206 |
| 960.415 | 27.61344 | 961.225 | 4.63609 | 961.184 | 6.13471 | 961.184 | 4.28604 | 961.184 | -1.18899 | 961.184 | 172.1055 | 961.184 | 71.62929 |  | 961.184 | 152.5007 |
| 961.116 | 27.6957 | 961.925 | 6.23136 | 961.885 | 5.23023 | 961.885 | 3.23674 | 961.885 | -1.52723 | 961.885 | 172.9696 | 961.885 | 72.89335 |  | 961.885 | 152.8482 |
| 961.817 | 27.77892 | 962.625 | 7.44291 | 962.585 | 4.85763 | 962.585 | 1.7126 | 962.585 | -1.16216 | 962.585 | 173.3562 | 962.585 | 74.85841 |  | 962.585 | 153.7257 |
| 962.519 | 27.86289 | 963.326 | 7.439 | 963.285 | 4.31452 | 963.285 | 0.33756 | 963.285 | -1.08471 | 963.285 | 173.8918 | 963.285 | 76.53586 |  | 963.285 | 154.4328 |
| 963.221 | 27.94733 | 964.026 | 6.98991 | 963.987 | 4.47955 | 963.987 | -0.28809 | 963.987 | -0.86636 | 963.987 | 175.1823 | 963.987 | 78.35878 |  | 963.987 | 155.8515 |
| 963.921 | 28.03227 | 964.725 | 6.16191 | 964.687 | 3.02764 | 964.687 | -0.67546 | 964.687 | -0.7685 | 964.687 | 176.7056 | 964.687 | 80.05664 |  | 964.687 | 155.6498 |
| 964.622 | 28.11772 | 965.425 | 5.68218 | 965.387 | 2.25723 | 965.387 | -0.02663 | 965.387 | -1.84151 | 965.387 | 179.2651 | 965.387 | 80.58363 |  | 965.387 | 156.1295 |
| 965.324 | 28.20325 | 966.125 | 5.12009 | 966.087 | 1.53451 | 966.087 | 0.65186 | 966.087 | -1.44006 | 966.087 | 181.8543 | 966.087 | 82.58508 |  | 966.087 | 156.657 |
| 966.024 | 28.28884 | 966.825 | 4.84636 | 966.787 | 1.079 | 966.787 | 0.5248 | 966.787 | 0 | 966.787 | 183.638 | 966.787 | 85.62514 |  | 966.787 | 157.4516 |
| 966.725 | 28.37439 | 967.524 | 5.60009 | 967.487 | 0.69556 | 967.487 | 0.01315 | 967.487 | 3.07017 | 967.487 | 185.037 | 967.487 | 87.44178 |  | 967.487 | 158.3183 |
| 967.426 | 28.4594 | 968.224 | 4.31082 | 968.188 | 0 | 968.188 | 0 | 968.188 | 5.83581 | 968.188 | 186.9373 | 968.188 | 88.9521 |  | 968.188 | 158.8747 |
| 968.126 | 28.54334 | 968.924 | 4.87764 | 968.888 | 2.97798 | 968.888 | 3.09064 | 968.888 | 8.88106 | 968.888 | 188.8204 | 968.888 | 90.74382 |  | 968.888 | 160.5365 |
| 968.827 | 28.62592 | 969.624 | 5.63609 | 969.587 | 6.06227 | 969.587 | 6.69107 | 969.587 | 11.69569 | 969.587 | 191.215 | 969.587 | 92.30671 |  | 969.587 | 162.3064 |
| 969.528 | 28.70676 | 970.323 | 6.58864 | 970.287 | 9.22734 | 970.287 | 8.8935 | 970.287 | 13.65233 | 970.287 | 192.2099 | 970.287 | 93.00982 |  | 970.287 | 164.1553 |
| 970.228 | 28.78586 | 971.023 | 7.87318 | 970.986 | 12.2318 | 970.986 | 11.539 | 970.986 | 19.29741 | 970.986 | 193.6496 | 970.986 | 97.40316 |  | 970.986 | 165.8454 |
| 970.929 | 28.86296 | 971.721 | 6.87818 | 971.686 | 14.57609 | 971.686 | 15.58555 | 971.686 | 23.80027 | 971.686 | 196.4886 | 971.686 | 100.6525 |  | 971.686 | 166.8735 |
| 971.63 | 28.9378 | 972.42 | 5.21 | 972.385 | 16.20295 | 972.385 | 19.87561 | 972.385 | 27.16368 | 972.385 | 199.5728 | 972.385 | 102.7642 |  | 972.385 | 167.186 |
| 972.329 | 29.00988 | 973.12 | 4.96782 | 973.086 | 19.78562 | 973.086 | 24.95842 | 973.086 | 29.62854 | 973.086 | 203.4464 | 973.086 | 103.9737 |  | 973.086 | 169.4506 |
| 973.03 | 29.07918 | 973.819 | 4.40318 | 973.785 | 23.62661 | 973.785 | 28.55887 | 973.785 | 34.91934 | 973.785 | 205.841 | 973.785 | 108.0128 |  | 973.785 | 171.9772 |
| 973.73 | 29.1455 | 974.518 | 4.89964 | 974.484 | 26.52728 | 974.484 | 30.73607 | 974.484 | 40.26272 | 974.484 | 206.8124 | 974.484 | 112.1044 |  | 974.484 | 173.5636 |
| 974.43 | 29.20875 | 975.217 | 4.24245 | 975.184 | 30.459 | 975.184 | 33.56024 | 975.184 | 44.00768 | 975.184 | 208.429 | 975.184 | 114.5958 |  | 975.184 | 176.1791 |
| 975.13 | 29.26869 | 975.916 | 3.97627 | 975.883 | 34.54775 | 975.883 | 38.11865 | 975.883 | 49.85931 | 975.883 | 211.7816 | 975.883 | 119.1957 |  | 975.883 | 178.9535 |
| 975.829 | 29.32546 | 976.614 | 3.81282 | 976.582 | 37.89269 | 976.582 | 41.4254 | 976.582 | 53.59928 | 976.582 | 213.8825 | 976.582 | 121.684 |  | 976.582 | 180.9841 |
| 976.529 | 29.37889 | 977.313 | 3.20764 | 977.281 | 42.57141 | 977.281 | 45.60319 | 977.281 | 57.90157 | 977.281 | 216.8545 | 977.281 | 124.7345 |  | 977.281 | 184.3484 |
| 977.23 | 29.42925 | 978.012 | 2.51564 | 977.981 | 46.54977 | 977.981 | 48.91026 | 977.981 | 62.29143 | 977.981 | 218.954 | 977.981 | 127.8709 |  | 977.981 | 187.0106 |
| 977.929 | 29.47621 | 978.711 | 1.19264 | 978.68 | 51.05952 | 978.68 | 52.81595 | 978.68 | 67.53675 | 978.68 | 221.6539 | 978.68 | 131.8644 |  | 978.68 | 190.206 |
| 978.629 | 29.51934 | 979.409 | 2.78973 | 979.378 | 55.05827 | 979.378 | 56.87431 | 979.378 | 72.93971 | 979.378 | 224.5082 | 979.378 | 136.0174 |  | 979.378 | 192.8923 |
| 979.329 | 29.55853 | 980.108 | 3.77227 | 980.077 | 58.7996 | 980.077 | 61.27059 | 980.077 | 78.05183 | 980.077 | 227.6986 | 980.077 | 139.8778 |  | 980.077 | 195.3193 |
| 980.028 | 29.59396 | 980.807 | 5.96709 | 980.776 | 62.60827 | 980.776 | 66.23028 | 980.776 | 83.9081 | 980.776 | 231.4525 | 980.776 | 144.4824 |  | 980.776 | 197.8136 |
| 980.727 | 29.62573 | 981.504 | 5.80173 | 981.474 | 66.48299 | 981.474 | 71.00676 | 981.474 | 90.6183 | 981.474 | 235.0249 | 981.474 | 149.9426 |  | 981.474 | 200.3759 |
| 981.426 | 29.65383 | 982.202 | 5.199 | 982.173 | 70.54423 | 982.173 | 76.8102 | 982.173 | 97.32968 | 982.173 | 239.6225 | 982.173 | 155.4023 |  | 982.173 | 203.1228 |
| 982.126 | 29.67802 | 982.901 | 6.025 | 982.871 | 75.44453 | 982.871 | 81.99755 | 982.871 | 102.4126 | 982.871 | 243.6058 | 982.871 | 159.2352 |  | 982.871 | 206.7106 |
| 982.826 | 29.69837 | 983.599 | 8.37982 | 983.57 | 80.00415 | 983.57 | 87.1678 | 983.57 | 107.5763 | 983.57 | 247.5702 | 983.57 | 163.1472 |  | 983.57 | 209.9559 |
| 983.524 | 29.71484 | 984.297 | 8.19182 | 984.268 | 84.04296 | 984.268 | 92.21641 | 984.268 | 114.5759 | 984.268 | 251.4147 | 984.268 | 168.8968 |  | 984.268 | 212.6822 |
| 984.224 | 29.72737 | 984.994 | 9.22882 | 984.966 | 88.88961 | 984.966 | 96.80541 | 984.966 | 121.3174 | 984.966 | 254.7996 | 984.966 | 174.3884 |  | 984.966 | 216.2164 |
| 984.922 | 29.73632 | 985.692 | 9.50491 | 985.666 | 93.71415 | 985.666 | 101.9677 | 985.666 | 126.6833 | 985.666 | 258.7544 | 985.666 | 178.5007 |  | 985.666 | 219.7247 |
| 985.621 | 29.7415 | 986.39 | 10.05636 | 986.364 | 96.42307 | 986.364 | 105.5372 | 986.364 | 131.0597 | 986.364 | 261.1198 | 986.364 | 181.6272 |  | 986.364 | 221.1212 |
| 986.319 | 29.74271 | 987.088 | 10.82582 | 987.062 | 99.49043 | 987.062 | 110.3471 | 987.062 | 136.6429 | 987.062 | 264.7256 | 987.062 | 185.9604 |  | 987.062 | 222.8761 |
| 987.019 | 29.74006 | 987.786 | 11.876 | 987.76 | 103.2766 | 987.76 | 114.6783 | 987.76 | 141.7892 | 987.76 | 267.8527 | 987.76 | 189.8568 |  | 987.76 | 225.3498 |
| 987.718 | 29.73379 | 988.483 | 11.58718 | 988.458 | 106.4311 | 988.458 | 118.3924 | 988.458 | 147.5358 | 988.458 | 270.3627 | 988.458 | 194.3535 |  | 988.458 | 227.1918 |
| 988.416 | 29.72414 | 989.181 | 14.58727 | 989.155 | 109.9656 | 989.155 | 123.1766 | 989.155 | 153.7944 | 989.155 | 273.9446 | 989.155 | 199.3639 |  | 989.155 | 229.4158 |
| 989.115 | 29.71119 | 989.879 | 15.12018 | 989.853 | 112.5116 | 989.853 | 127.305 | 989.853 | 158.783 | 989.853 | 276.8689 | 989.853 | 203.1026 |  | 989.853 | 230.6493 |
| 989.813 | 29.6951 | 990.576 | 16.51564 | 990.551 | 115.611 | 990.551 | 129.0471 | 990.551 | 163.5329 | 990.551 | 277.4069 | 990.551 | 206.6026 |  | 990.551 | 232.4363 |
| 990.512 | 29.67578 | 991.274 | 16.39509 | 991.248 | 118.0186 | 991.248 | 132.0568 | 991.248 | 167.2525 | 991.248 | 279.2142 | 991.248 | 209.074 |  | 991.248 | 233.5332 |
| 991.21 | 29.6536 | 991.97 | 18.16645 | 991.946 | 120.7226 | 991.946 | 135.4496 | 991.946 | 169.9706 | 991.946 | 281.4029 | 991.946 | 210.5421 |  | 991.946 | 234.9248 |
| 991.909 | 29.62869 | 992.668 | 19.372 | 992.643 | 121.4354 | 992.643 | 138.0979 | 992.643 | 174.2984 | 992.643 | 282.8489 | 992.643 | 213.6218 |  | 992.643 | 234.3271 |
| 992.607 | 29.60082 | 993.365 | 21.69464 | 993.341 | 122.6896 | 993.341 | 139.7993 | 993.341 | 177.4894 | 993.341 | 283.3462 | 993.341 | 215.5628 |  | 993.341 | 234.2688 |
| 993.305 | 29.57009 | 994.062 | 22.27145 | 994.038 | 123.4929 | 994.038 | 140.6373 | 994.038 | 180.5916 | 994.038 | 282.9818 | 994.038 | 217.4169 |  | 994.038 | 233.7615 |
| 994.003 | 29.53707 | 994.758 | 23.43636 | 994.736 | 124.9438 | 994.736 | 140.8012 | 994.736 | 185.4471 | 994.736 | 281.9417 | 994.736 | 221.0224 |  | 994.736 | 233.9 |
| 994.701 | 29.50199 | 995.456 | 27.35927 | 995.433 | 125.8001 | 995.433 | 141.3785 | 995.433 | 188.9374 | 995.433 | 281.3165 | 995.433 | 223.2646 |  | 995.433 | 233.4457 |
| 995.399 | 29.46503 | 996.153 | 30.77564 | 996.13 | 127.4166 | 996.13 | 142.2627 | 996.13 | 190.0783 | 996.13 | 280.9984 | 996.13 | 223.1573 |  | 996.13 | 233.7516 |
| 996.096 | 29.42605 | 996.85 | 38.04173 | 996.827 | 128.5504 | 996.827 | 142.5696 | 996.827 | 191.1036 | 996.827 | 280.1029 | 996.827 | 222.9344 |  | 996.827 | 233.5748 |
| 996.795 | 29.38519 | 997.546 | 48.29655 | 997.524 | 128.463 | 997.524 | 144.6494 | 997.524 | 192.4869 | 997.524 | 280.9803 | 997.524 | 223.0696 |  | 997.524 | 232.1768 |
| 997.492 | 29.34263 | 998.242 | 59.13291 | 998.221 | 127.7005 | 998.221 | 145.6588 | 998.221 | 193.5053 | 998.221 | 280.7874 | 998.221 | 222.8398 |  | 998.221 | 230.1038 |
| 998.19 | 29.29846 | 998.939 | 67.29209 | 998.918 | 128.47 | 998.918 | 146.4731 | 998.918 | 193.3271 | 998.918 | 280.3993 | 998.918 | 221.4134 |  | 998.918 | 229.5627 |
| 998.887 | 29.25268 | 999.636 | 72.05691 | 999.615 | 128.9662 | 999.615 | 146.9615 | 999.615 | 194.2632 | 999.615 | 279.6854 | 999.615 | 221.1014 |  | 999.615 | 228.7483 |
| 999.585 | 29.20524 | 1000.33 | 73.88536 | 1000.31 | 129.9536 | 1000.31 | 147.0896 | 1000.31 | 195.7971 | 1000.31 | 278.6146 | 1000.31 | 221.3907 |  | 1000.31 | 228.4289 |
| 1000.28 | 29.15624 | 1001.03 | 76.32709 | 1001.01 | 130.6113 | 1001.01 | 146.5303 | 1001.01 | 197.1428 | 1001.01 | 276.8477 | 1001.01 | 221.4829 |  | 1001.01 | 227.7704 |
| 1000.98 | 29.10589 | 1001.72 | 79.01155 | 1001.7 | 130.6888 | 1001.7 | 146.1349 | 1001.7 | 198.3088 | 1001.7 | 275.262 | 1001.7 | 221.4133 |  | 1001.7 | 226.5505 |
| 1001.68 | 29.05428 | 1002.42 | 79.03727 | 1002.4 | 130.2726 | 1002.4 | 146.8359 | 1002.4 | 198.4751 | 1002.4 | 274.7555 | 1002.4 | 220.3261 |  | 1002.4 | 224.818 |
| 1002.37 | 29.00162 | 1003.12 | 74.68173 | 1003.1 | 129.6167 | 1003.1 | 146.9089 | 1003.1 | 199.1968 | 1003.1 | 273.6209 | 1003.1 | 219.7942 |  | 1003.1 | 222.8459 |
| 1003.07 | 28.94788 | 1003.81 | 71.011 | 1003.79 | 129.096 | 1003.79 | 145.3506 | 1003.79 | 199.9177 | 1003.79 | 270.8723 | 1003.79 | 219.2795 |  | 1003.79 | 221.0278 |
| 1003.77 | 28.89277 | 1004.51 | 61.77564 | 1004.49 | 128.2482 | 1004.49 | 144.2118 | 1004.49 | 200.5794 | 1004.49 | 268.526 | 1004.49 | 218.6876 |  | 1004.49 | 218.8637 |
| 1004.47 | 28.83595 | 1005.2 | 52.84691 | 1005.19 | 127.9202 | 1005.19 | 143.3544 | 1005.19 | 200.0485 | 1005.19 | 266.4611 | 1005.19 | 216.9032 |  | 1005.19 | 217.2195 |
| 1005.16 | 28.7773 | 1005.9 | 42.20473 | 1005.88 | 127.3851 | 1005.88 | 143.5188 | 1005.88 | 199.375 | 1005.88 | 265.4351 | 1005.88 | 214.9941 |  | 1005.88 | 215.387 |
| 1005.86 | 28.71653 | 1006.6 | 33.52409 | 1006.58 | 126.8651 | 1006.58 | 142.6686 | 1006.58 | 197.8752 | 1006.58 | 263.3775 | 1006.58 | 212.2408 |  | 1006.58 | 213.5508 |
| 1006.56 | 28.65335 | 1007.29 | 26.91336 | 1007.28 | 125.8253 | 1007.28 | 141.3165 | 1007.28 | 196.6855 | 1007.28 | 260.8178 | 1007.28 | 209.7975 |  | 1007.28 | 211.1948 |
| 1007.25 | 28.58786 | 1007.99 | 23.13055 | 1007.97 | 124.8675 | 1007.97 | 138.9934 | 1007.97 | 196.5357 | 1007.97 | 257.3044 | 1007.97 | 208.4122 |  | 1007.97 | 208.9396 |
| 1007.95 | 28.5203 | 1008.68 | 17.99582 | 1008.67 | 123.5759 | 1008.67 | 135.2081 | 1008.67 | 195.8704 | 1008.67 | 252.3116 | 1008.67 | 206.4933 |  | 1008.67 | 206.3318 |
| 1008.65 | 28.45077 | 1009.38 | 11.94373 | 1009.36 | 121.9698 | 1009.36 | 132.3255 | 1009.36 | 193.2879 | 1009.36 | 248.2387 | 1009.36 | 202.6752 |  | 1009.36 | 203.4282 |
| 1009.34 | 28.3795 | 1010.07 | 10.04109 | 1010.06 | 119.8085 | 1010.06 | 131.7075 | 1010.06 | 190.7771 | 1010.06 | 246.4131 | 1010.06 | 198.9109 |  | 1010.06 | 199.9508 |
| 1010.04 | 28.30629 | 1010.77 | 9.00409 | 1010.76 | 116.6161 | 1010.76 | 130.2598 | 1010.76 | 188.9088 | 1010.76 | 243.7579 | 1010.76 | 195.789 |  | 1010.76 | 195.4421 |
| 1010.74 | 28.23119 | 1011.47 | 6.65391 | 1011.45 | 113.3874 | 1011.45 | 127.993 | 1011.45 | 184.6847 | 1011.45 | 240.3008 | 1011.45 | 190.3293 |  | 1011.45 | 190.916 |
| 1011.43 | 28.1545 | 1012.16 | 4.99664 | 1012.15 | 111.1579 | 1012.15 | 125.7616 | 1012.15 | 181.0987 | 1012.15 | 236.8618 | 1012.15 | 185.4898 |  | 1012.15 | 187.3702 |
| 1012.13 | 28.07757 | 1012.86 | 0.77309 | 1012.84 | 107.445 | 1012.84 | 122.9026 | 1012.84 | 177.5696 | 1012.84 | 232.8126 | 1012.84 | 180.725 |  | 1012.84 | 182.3599 |
| 1012.82 | 28.00055 | 1013.55 | -2.21373 | 1013.54 | 103.6078 | 1013.54 | 120.6523 | 1013.54 | 172.9106 | 1013.54 | 229.3547 | 1013.54 | 174.8125 |  | 1013.54 | 177.2065 |
| 1013.52 | 27.92398 | 1014.25 | -4.73882 | 1014.23 | 99.72114 | 1014.23 | 117.1745 | 1014.23 | 168.3388 | 1014.23 | 224.6866 | 1014.23 | 169.0051 |  | 1014.23 | 172.0225 |
| 1014.22 | 27.84694 | 1014.94 | -6.04055 | 1014.93 | 96.61971 | 1014.93 | 113.8076 | 1014.93 | 163.7501 | 1014.93 | 220.1121 | 1014.93 | 163.1629 |  | 1014.93 | 167.6048 |
| 1014.91 | 27.76934 | 1015.64 | -8.17755 | 1015.62 | 93.68223 | 1015.62 | 111.3499 | 1015.62 | 159.2441 | 1015.62 | 216.4642 | 1015.62 | 157.4212 |  | 1015.62 | 163.3699 |
| 1015.61 | 27.6913 | 1016.33 | -8.54582 | 1016.32 | 89.95277 | 1016.32 | 107.754 | 1016.32 | 153.022 | 1016.32 | 211.6607 | 1016.32 | 149.9456 |  | 1016.32 | 158.3242 |
| 1016.3 | 27.61309 | 1017.03 | -6.84691 | 1017.01 | 85.9554 | 1017.01 | 102.8776 | 1017.01 | 146.7817 | 1017.01 | 205.594 | 1017.01 | 142.4697 |  | 1017.01 | 153.0295 |
| 1017 | 27.53512 | 1017.72 | -9.02755 | 1017.71 | 81.59625 | 1017.71 | 98.16177 | 1017.71 | 140.5291 | 1017.71 | 199.6707 | 1017.71 | 134.9636 |  | 1017.71 | 147.3541 |
| 1017.7 | 27.45775 | 1018.41 | -10.392 | 1018.4 | 76.42404 | 1018.4 | 93.04523 | 1018.4 | 134.3026 | 1018.4 | 193.3639 | 1018.4 | 127.5014 |  | 1018.4 | 140.8845 |
| 1018.39 | 27.38088 | 1019.11 | -10.0759 | 1019.1 | 71.73189 | 1019.1 | 87.52584 | 1019.1 | 128.8235 | 1019.1 | 186.6369 | 1019.1 | 120.7688 |  | 1019.1 | 134.8761 |
| 1019.09 | 27.30447 | 1019.8 | -9.074 | 1019.79 | 67.07956 | 1019.79 | 83.33057 | 1019.79 | 122.7016 | 1019.79 | 181.2514 | 1019.79 | 113.4113 |  | 1019.79 | 128.9263 |
| 1019.78 | 27.22855 | 1020.5 | -7.66591 | 1020.49 | 62.54044 | 1020.49 | 79.07008 | 1020.49 | 115.5123 | 1020.49 | 175.7833 | 1020.49 | 104.9685 |  | 1020.49 | 123.071 |
| 1020.48 | 27.15328 | 1021.19 | -7.53345 | 1021.18 | 57.1384 | 1021.18 | 74.30136 | 1021.18 | 108.8022 | 1021.18 | 169.8243 | 1021.18 | 97.02272 |  | 1021.18 | 116.3715 |
| 1021.17 | 27.07881 | 1021.89 | -7.02536 | 1021.88 | 53.00438 | 1021.88 | 70.13048 | 1021.88 | 104.9607 | 1021.88 | 164.4459 | 1021.88 | 91.92774 |  | 1021.88 | 110.9213 |
| 1021.87 | 27.00527 | 1022.58 | -6.18927 | 1022.57 | 48.7938 | 1022.57 | 64.98871 | 1022.57 | 99.7235 | 1022.57 | 158.1138 | 1022.57 | 85.45489 |  | 1022.57 | 105.4133 |
| 1022.56 | 26.93248 | 1023.28 | -8.183 | 1023.27 | 44.38564 | 1023.27 | 60.4176 | 1023.27 | 93.86199 | 1023.27 | 152.3352 | 1023.27 | 78.33985 |  | 1023.27 | 99.68892 |
| 1023.26 | 26.86043 | 1023.97 | -8.994 | 1023.96 | 40.94819 | 1023.96 | 56.0119 | 1023.96 | 87.85555 | 1023.96 | 146.7392 | 1023.96 | 71.09778 |  | 1023.96 | 94.95406 |
| 1023.95 | 26.78948 | 1024.66 | -10.335 | 1024.65 | 37.39456 | 1024.65 | 51.63786 | 1024.65 | 83.69652 | 1024.65 | 141.1749 | 1024.65 | 65.70314 |  | 1024.65 | 90.10301 |
| 1024.65 | 26.71988 | 1025.36 | -10.2706 | 1025.35 | 34.06668 | 1025.35 | 46.82272 | 1025.35 | 78.40206 | 1025.35 | 135.1522 | 1025.35 | 59.15514 |  | 1025.35 | 85.45891 |
| 1025.34 | 26.65156 | 1026.05 | -10.371 | 1026.04 | 31.82666 | 1026.04 | 44.13346 | 1026.04 | 73.10362 | 1026.04 | 131.2726 | 1026.04 | 52.62108 |  | 1026.04 | 81.92148 |
| 1026.04 | 26.58481 | 1026.74 | -10.6515 | 1026.74 | 29.47427 | 1026.74 | 41.13087 | 1026.74 | 68.6133 | 1026.74 | 127.0625 | 1026.74 | 46.87723 |  | 1026.74 | 78.25287 |
| 1026.73 | 26.51948 | 1027.44 | -11.5346 | 1027.43 | 26.71661 | 1027.43 | 38.58103 | 1027.43 | 66.57567 | 1027.43 | 123.3224 | 1027.43 | 43.60399 |  | 1027.43 | 74.19779 |
| 1027.43 | 26.45568 | 1028.13 | -11.9048 | 1028.12 | 25.38805 | 1028.12 | 35.89048 | 1028.12 | 62.9645 | 1028.12 | 119.4415 | 1028.12 | 38.75719 |  | 1028.12 | 71.57181 |
| 1028.12 | 26.39341 | 1028.82 | -12.1438 | 1028.82 | 23.85152 | 1028.82 | 34.15197 | 1028.82 | 59.58142 | 1028.82 | 116.4955 | 1028.82 | 34.12058 |  | 1028.82 | 68.71906 |
| 1028.82 | 26.33249 | 1029.52 | -12.3045 | 1029.51 | 23.35787 | 1029.51 | 32.43025 | 1029.51 | 56.70106 | 1029.51 | 113.5835 | 1029.51 | 30.0046 |  | 1029.51 | 66.92799 |
| 1029.51 | 26.27292 | 1030.21 | -11.3207 | 1030.21 | 22.0484 | 1030.21 | 31.48606 | 1030.21 | 54.48213 | 1030.21 | 111.4317 | 1030.21 | 26.53214 |  | 1030.21 | 64.3023 |
| 1030.21 | 26.2152 | 1030.9 | -9.48755 | 1030.9 | 19.34502 | 1030.9 | 31.17913 | 1030.9 | 52.30098 | 1030.9 | 109.9345 | 1030.9 | 23.11537 |  | 1030.9 | 60.30151 |
| 1030.9 | 26.15945 | 1031.6 | -8.76691 | 1031.59 | 17.08683 | 1031.59 | 29.46208 | 1031.59 | 51.55472 | 1031.59 | 107.0272 | 1031.59 | 21.13349 |  | 1031.59 | 56.74591 |
| 1031.6 | 26.10556 | 1032.29 | -7.74155 | 1032.29 | 13.94902 | 1032.29 | 28.42562 | 1032.29 | 50.56304 | 1032.29 | 104.7832 | 1032.29 | 18.88828 |  | 1032.29 | 52.29187 |
| 1032.29 | 26.05364 | 1032.98 | -6.07482 | 1032.98 | 13.19436 | 1032.98 | 25.05641 | 1032.98 | 48.81662 | 1032.98 | 100.2237 | 1032.98 | 15.90623 |  | 1032.98 | 50.23979 |
| 1032.98 | 26.00367 | 1033.68 | -5.96982 | 1033.67 | 12.61441 | 1033.67 | 22.61976 | 1033.67 | 46.65746 | 1033.67 | 96.59674 | 1033.67 | 12.51145 |  | 1033.67 | 48.36243 |
| 1033.68 | 25.95568 | 1034.37 | -6.68209 | 1034.37 | 11.88942 | 1034.37 | 20.62965 | 1034.37 | 46.4156 | 1034.37 | 93.3991 | 1034.37 | 11.01607 |  | 1034.37 | 46.32122 |
| 1034.37 | 25.90954 | 1035.06 | -7.01645 | 1035.06 | 10.64897 | 1035.06 | 19.10191 | 1035.06 | 44.03859 | 1035.06 | 90.68106 | 1035.06 | 7.40344 |  | 1035.06 | 43.78335 |
| 1035.07 | 25.86529 | 1035.76 | -6.39164 | 1035.76 | 9.72306 | 1035.76 | 17.67953 | 1035.76 | 41.19908 | 1035.76 | 88.05114 | 1035.76 | 3.3104 |  | 1035.76 | 41.54122 |
| 1035.76 | 25.823 | 1036.45 | -6.43055 | 1036.45 | 8.17146 | 1036.45 | 16.21579 | 1036.45 | 38.98364 | 1036.45 | 85.39711 | 1036.45 | -0.14067 |  | 1036.45 | 38.69221 |
| 1036.45 | 25.78237 | 1037.14 | -8.90009 | 1037.14 | 5.97012 | 1037.14 | 14.59585 | 1037.14 | 36.16955 | 1037.14 | 82.58688 | 1037.14 | -4.19038 |  | 1037.14 | 35.19345 |
| 1037.15 | 25.74324 | 1037.83 | -12.454 | 1037.83 | 5.12943 | 1037.83 | 11.60897 | 1037.83 | 33.90394 | 1037.83 | 78.40971 | 1037.83 | -7.69161 |  | 1037.83 | 33.05534 |
| 1037.84 | 25.7058 | 1038.53 | -12.628 | 1038.53 | 5.32289 | 1038.53 | 10.03158 | 1038.53 | 32.32308 | 1038.53 | 75.62478 | 1038.53 | -10.526 |  | 1038.53 | 31.93258 |
| 1038.53 | 25.67029 | 1039.22 | -13.4487 | 1039.22 | 4.75163 | 1039.22 | 9.22164 | 1039.22 | 30.68413 | 1039.22 | 73.62455 | 1039.22 | -13.4006 |  | 1039.22 | 30.06391 |
| 1039.23 | 25.6364 | 1039.91 | -14.0839 | 1039.91 | 4.06495 | 1039.91 | 8.11434 | 1039.91 | 27.82438 | 1039.91 | 71.32695 | 1039.91 | -17.4959 |  | 1039.91 | 28.07981 |
| 1039.92 | 25.60428 | 1040.6 | -15.4764 | 1040.6 | 3.11177 | 1040.6 | 5.47121 | 1040.6 | 24.95876 | 1040.6 | 67.49354 | 1040.6 | -21.5972 |  | 1040.6 | 25.82922 |
| 1040.62 | 25.5736 | 1041.3 | -17.0684 | 1041.3 | 2.10942 | 1041.3 | 2.33314 | 1041.3 | 21.53162 | 1041.3 | 63.14792 | 1041.3 | -26.2779 |  | 1041.3 | 23.51065 |
| 1041.31 | 25.54451 | 1041.99 | -17.5896 | 1041.99 | 0.20785 | 1041.99 | 0.22356 | 1041.99 | 18.4958 | 1041.99 | 59.84805 | 1041.99 | -30.5493 |  | 1041.99 | 20.31166 |
| 1042 | 25.51698 | 1042.68 | -18.5108 | 1042.68 | -0.92474 | 1042.68 | -0.45282 | 1042.68 | 15.75038 | 1042.68 | 57.98139 | 1042.68 | -34.5303 |  | 1042.68 | 17.88166 |
| 1042.7 | 25.49028 | 1043.37 | -20.8179 | 1043.37 | -2.43961 | 1043.37 | -1.08395 | 1043.37 | 11.95455 | 1043.37 | 56.15996 | 1043.37 | -39.5618 |  | 1043.37 | 15.06937 |
| 1043.39 | 25.46444 | 1044.06 | -21.2354 | 1044.07 | -4.10022 | 1044.07 | -1.76875 | 1044.07 | 10.47115 | 1044.07 | 54.26762 | 1044.07 | -42.2987 |  | 1044.07 | 12.09254 |
| 1044.08 | 25.43933 | 1044.76 | -18.3834 | 1044.76 | -7.03074 | 1044.76 | -2.00222 | 1044.76 | 8.80473 | 1044.76 | 52.84386 | 1044.76 | -45.2008 |  | 1044.76 | 7.8646 |
| 1044.77 | 25.41486 | 1045.45 | -16.3016 | 1045.45 | -8.08886 | 1045.45 | -3.71996 | 1045.45 | 5.54874 | 1045.45 | 49.93584 | 1045.45 | -49.6924 |  | 1045.45 | 5.50906 |
| 1045.47 | 25.39116 | 1046.14 | -16.0126 | 1046.14 | -7.95983 | 1046.14 | -5.90644 | 1046.14 | 3.55038 | 1046.14 | 46.55906 | 1046.14 | -52.9264 |  | 1046.14 | 4.34068 |
| 1046.16 | 25.36782 | 1046.83 | -16.2869 | 1046.84 | -9.32931 | 1046.84 | -6.90789 | 1046.84 | 1.74309 | 1046.84 | 44.35007 | 1046.84 | -55.9872 |  | 1046.84 | 1.65498 |
| 1046.85 | 25.34489 | 1047.52 | -17.6508 | 1047.53 | -11.3727 | 1047.53 | -6.99516 | 1047.53 | 0.49966 | 1047.53 | 43.07251 | 1047.53 | -58.4662 |  | 1047.53 | -1.68584 |
| 1047.55 | 25.32227 | 1048.22 | -17.8033 | 1048.22 | -11.1047 | 1048.22 | -7.67639 | 1048.22 | -1.04339 | 1048.22 | 41.20099 | 1048.22 | -61.2449 |  | 1048.22 | -2.71523 |
| 1048.24 | 25.29972 | 1048.91 | -17.1736 | 1048.91 | -11.0061 | 1048.91 | -8.65149 | 1048.91 | -1.98467 | 1048.91 | 39.0356 | 1048.91 | -63.4218 |  | 1048.91 | -3.91406 |
| 1048.93 | 25.27751 | 1049.6 | -16.2646 | 1049.6 | -10.4293 | 1049.6 | -8.86005 | 1049.6 | -2.33515 | 1049.6 | 37.63675 | 1049.6 | -65.0079 |  | 1049.6 | -4.63467 |
| 1049.62 | 25.25591 | 1050.29 | -15.8966 | 1050.3 | -11.0589 | 1050.3 | -9.82866 | 1050.3 | -2.41637 | 1050.3 | 35.4606 | 1050.3 | -66.3427 |  | 1050.3 | -6.58052 |
| 1050.32 | 25.23482 | 1050.98 | -14.5071 | 1050.99 | -12.5233 | 1050.99 | -11.8792 | 1050.99 | -2.66862 | 1050.99 | 32.2198 | 1050.99 | -67.8305 |  | 1050.99 | -9.34228 |
| 1051.01 | 25.21417 | 1051.67 | -15.8647 | 1051.68 | -13.1012 | 1051.68 | -12.4912 | 1051.68 | -2.22557 | 1051.68 | 30.4175 | 1051.68 | -68.6231 |  | 1051.68 | -11.2176 |
| 1051.7 | 25.19396 | 1052.36 | -18.392 | 1052.37 | -12.9518 | 1052.37 | -12.0117 | 1052.37 | -3.32959 | 1052.37 | 29.70672 | 1052.37 | -70.9627 |  | 1052.37 | -12.3656 |
| 1052.39 | 25.1744 | 1053.05 | -20.0238 | 1053.06 | -12.3839 | 1053.06 | -11.7527 | 1053.06 | -2.65732 | 1053.06 | 28.77541 | 1053.06 | -71.5261 |  | 1053.06 | -13.0952 |
| 1053.08 | 25.15535 | 1053.75 | -20.78 | 1053.75 | -13.2811 | 1053.75 | -11.6502 | 1053.75 | -2.82449 | 1053.75 | 27.68758 | 1053.75 | -72.9289 |  | 1053.75 | -15.2898 |
| 1053.78 | 25.13698 | 1054.44 | -21.3914 | 1054.44 | -12.5195 | 1054.44 | -10.7312 | 1054.44 | -3.1954 | 1054.44 | 27.41631 | 1054.44 | -74.5354 |  | 1054.44 | -15.8255 |
| 1054.47 | 25.11906 | 1055.13 | -22.0737 | 1055.14 | -11.3543 | 1055.14 | -11.5243 | 1055.14 | -3.60369 | 1055.14 | 25.41568 | 1055.14 | -76.1972 |  | 1055.14 | -15.9766 |
| 1055.16 | 25.10162 | 1055.82 | -22.6011 | 1055.83 | -10.2603 | 1055.83 | -10.9481 | 1055.83 | -2.07321 | 1055.83 | 24.8016 | 1055.83 | -75.9024 |  | 1055.83 | -16.18 |
| 1055.85 | 25.08473 | 1056.51 | -21.5246 | 1056.52 | -9.86483 | 1056.52 | -9.86684 | 1056.52 | -1.32471 | 1056.52 | 24.69255 | 1056.52 | -76.3895 |  | 1056.52 | -17.082 |
| 1056.54 | 25.06857 | 1057.2 | -22.7193 | 1057.21 | -9.86923 | 1057.21 | -9.18945 | 1057.21 | -2.12345 | 1057.21 | 24.17966 | 1057.21 | -78.4239 |  | 1057.21 | -18.3838 |
| 1057.24 | 25.05297 | 1057.89 | -21.9076 | 1057.9 | -9.28836 | 1057.9 | -8.37689 | 1057.9 | -1.75355 | 1057.9 | 23.80192 | 1057.9 | -79.2896 |  | 1057.9 | -19.1004 |
| 1057.93 | 25.03789 | 1058.58 | -21.7042 | 1058.59 | -8.61889 | 1058.59 | -7.16918 | 1058.59 | -1.81345 | 1058.59 | 23.81935 | 1058.59 | -80.5851 |  | 1058.59 | -19.7283 |
| 1058.62 | 25.02317 | 1059.27 | -19.704 | 1059.28 | -7.95975 | 1059.28 | -6.63876 | 1059.28 | -1.81238 | 1059.28 | 23.15947 | 1059.28 | -81.8197 |  | 1059.28 | -20.3666 |
| 1059.31 | 25.00852 | 1059.96 | -19.9538 | 1059.97 | -7.51888 | 1059.97 | -6.36907 | 1059.97 | -1.24483 | 1059.97 | 22.23887 | 1059.97 | -82.4877 |  | 1059.97 | -21.2231 |
| 1060 | 24.99409 | 1060.65 | -20.0141 | 1060.66 | -8.30744 | 1060.66 | -6.48696 | 1060.66 | -1.75277 | 1060.66 | 20.93069 | 1060.66 | -84.2313 |  | 1060.66 | -23.3091 |
| 1060.69 | 24.97998 | 1061.34 | -19.7873 | 1061.35 | -9.35563 | 1061.35 | -6.58891 | 1061.35 | 0.00988 | 1061.35 | 19.63846 | 1061.35 | -83.7043 |  | 1061.35 | -25.6547 |
| 1061.39 | 24.96595 | 1062.03 | -18.5881 | 1062.04 | -9.32573 | 1062.04 | -7.67973 | 1062.04 | 0.77484 | 1062.04 | 17.35735 | 1062.04 | -84.1749 |  | 1062.04 | -26.9222 |
| 1062.08 | 24.95198 | 1062.72 | -17.8958 | 1062.74 | -9.68085 | 1062.74 | -8.39713 | 1062.74 | 0.64082 | 1062.74 | 15.4324 | 1062.74 | -85.5625 |  | 1062.74 | -28.5936 |
| 1062.77 | 24.93811 | 1063.41 | -18.0316 | 1063.42 | -10.6722 | 1063.42 | -8.1831 | 1063.42 | -0.10275 | 1063.42 | 14.4734 | 1063.42 | -87.5238 |  | 1063.42 | -30.8636 |
| 1063.46 | 24.92406 | 1064.1 | -18.8776 | 1064.12 | -10.3774 | 1064.12 | -7.20175 | 1064.12 | 0.4593 | 1064.12 | 14.2472 | 1064.12 | -88.2152 |  | 1064.12 | -31.8849 |
| 1064.15 | 24.90966 | 1064.79 | -18.1114 | 1064.81 | -10.6225 | 1064.81 | -6.84711 | 1064.81 | 1.24772 | 1064.81 | 13.41155 | 1064.81 | -88.6624 |  | 1064.81 | -33.4275 |
| 1064.84 | 24.89502 | 1065.48 | -17.5224 | 1065.5 | -9.97567 | 1065.5 | -5.40085 | 1065.5 | 0.66909 | 1065.5 | 13.66752 | 1065.5 | -90.4767 |  | 1065.5 | -34.078 |
| 1065.53 | 24.88027 | 1066.17 | -17.6943 | 1066.19 | -9.27689 | 1066.19 | -6.37667 | 1066.19 | 0.61868 | 1066.19 | 11.50141 | 1066.19 | -91.7627 |  | 1066.19 | -34.6767 |
| 1066.22 | 24.86544 | 1066.86 | -19.1714 | 1066.88 | -7.83579 | 1066.88 | -4.41243 | 1066.88 | 0.28338 | 1066.88 | 12.27536 | 1066.88 | -93.3336 |  | 1066.88 | -34.533 |
| 1066.91 | 24.85039 | 1067.55 | -20.2257 | 1067.57 | -5.88284 | 1067.57 | -3.49399 | 1067.57 | -0.54353 | 1067.57 | 12.00351 | 1067.57 | -95.3962 |  | 1067.57 | -33.8775 |
| 1067.6 | 24.83541 | 1068.24 | -21.3046 | 1068.26 | -5.8608 | 1068.26 | -3.18757 | 1068.26 | -0.19204 | 1068.26 | 11.11964 | 1068.26 | -96.2803 |  | 1068.26 | -35.1528 |
| 1068.29 | 24.82068 | 1068.93 | -22.1975 | 1068.95 | -5.14448 | 1068.95 | -1.26421 | 1068.95 | -0.51491 | 1068.95 | 11.85271 | 1068.95 | -96.7793 |  | 1068.95 | -35.7339 |
| 1068.98 | 24.80606 | 1069.62 | -23.3337 | 1069.64 | -4.6423 | 1069.64 | 0.45973 | 1069.64 | -2.35651 | 1069.64 | 12.78681 | 1069.64 | -98.4235 |  | 1069.64 | -36.5292 |
| 1069.68 | 24.79127 | 1070.31 | -23.9289 | 1070.33 | -3.30466 | 1070.33 | 0.61735 | 1070.33 | -3.16281 | 1070.33 | 12.74314 | 1070.33 | -99.0323 |  | 1070.33 | -36.4889 |
| 1070.37 | 24.77582 | 1071 | -25.2123 | 1071.02 | -2.97278 | 1071.02 | 2.48191 | 1071.02 | -2.80484 | 1071.02 | 14.40641 | 1071.02 | -98.4769 |  | 1071.02 | -37.4545 |
| 1071.06 | 24.76 | 1071.69 | -25.0293 | 1071.7 | -0.61265 | 1071.7 | 2.79304 | 1071.7 | -3.51714 | 1071.7 | 14.51916 | 1071.7 | -98.9946 |  | 1071.7 | -36.373 |
| 1071.75 | 24.74383 | 1072.38 | -26.5177 | 1072.39 | 1.85568 | 1072.39 | 3.13145 | 1072.39 | -2.65622 | 1072.39 | 14.65629 | 1072.39 | -97.9362 |  | 1072.39 | -34.0216 |
| 1072.44 | 24.72727 | 1073.07 | -27.2303 | 1073.08 | 1.89555 | 1073.08 | 4.4308 | 1073.08 | -2.01888 | 1073.08 | 15.75434 | 1073.08 | -97.1014 |  | 1073.08 | -33.8606 |
| 1073.13 | 24.71034 | 1073.75 | -28.4951 | 1073.77 | 1.90024 | 1073.77 | 6.72062 | 1073.77 | -2.09078 | 1073.77 | 17.84287 | 1073.77 | -96.9758 |  | 1073.77 | -33.7347 |
| 1073.82 | 24.69298 | 1073.97 | -29.559 | 1074.46 | 0.26709 | 1074.46 | 6.89599 | 1074.46 | -1.70719 | 1074.46 | 17.81695 | 1074.46 | -96.3948 |  | 1074.46 | -35.2467 |
| 1074.51 | 24.67549 | 1074.66 | -27.5866 | 1075.15 | 0.04236 | 1075.15 | 6.75986 | 1075.15 | -0.89439 | 1075.15 | 17.47953 | 1075.15 | -95.3845 |  | 1075.15 | -35.3503 |
| 1075.2 | 24.65727 | 1075.35 | -25.8006 | 1075.84 | -1.08295 | 1075.84 | 9.78452 | 1075.84 | 1.54684 | 1075.84 | 20.3029 | 1075.84 | -92.7458 |  | 1075.84 | -36.3544 |
| 1075.89 | 24.63845 | 1076.04 | -26.4299 | 1076.53 | -2.03638 | 1076.53 | 11.40075 | 1076.53 | 4.55353 | 1076.53 | 21.71784 | 1076.53 | -89.5417 |  | 1076.53 | -37.1866 |
| 1076.58 | 24.6193 | 1076.73 | -27.4793 | 1077.22 | -1.84961 | 1077.22 | 11.17268 | 1077.22 | 6.72787 | 1077.22 | 21.28848 | 1077.22 | -87.1699 |  | 1077.22 | -36.8787 |
| 1077.27 | 24.60015 | 1077.42 | -26.0357 | 1077.91 | -0.74403 | 1077.91 | 12.23147 | 1077.91 | 8.35142 | 1077.91 | 22.14597 | 1077.91 | -85.3489 |  | 1077.91 | -35.6519 |
| 1077.96 | 24.58109 | 1078.11 | -26.5846 | 1078.6 | 0.08999 | 1078.6 | 12.65653 | 1078.6 | 11.83183 | 1078.6 | 22.36974 | 1078.6 | -81.671 |  | 1078.6 | -34.6967 |
| 1078.65 | 24.56157 | 1078.81 | -27.4993 | 1079.29 | -0.00509 | 1079.29 | 14.16259 | 1079.29 | 13.04985 | 1079.29 | 23.67451 | 1079.29 | -80.2555 |  | 1079.29 | -34.6706 |
| 1079.33 | 24.54164 | 1079.49 | -26.9383 | 1079.97 | 2.07629 | 1079.97 | 14.72671 | 1079.97 | 13.49015 | 1079.97 | 24.04026 | 1079.97 | -79.6206 |  | 1079.97 | -32.4698 |
| 1080.02 | 24.52104 | 1080.19 | -29.98 | 1080.66 | 2.45133 | 1080.66 | 15.7069 | 1080.66 | 16.43186 | 1080.66 | 24.81916 | 1080.66 | -76.4814 |  | 1080.66 | -31.9736 |
| 1080.71 | 24.49932 | 1080.88 | -29.2963 | 1081.35 | 2.28029 | 1081.35 | 18.082 | 1081.35 | 18.99122 | 1081.35 | 26.99297 | 1081.35 | -73.7246 |  | 1081.35 | -32.0235 |
| 1081.4 | 24.47652 | 1081.57 | -27.8596 | 1082.04 | 2.37779 | 1082.04 | 19.36907 | 1082.04 | 21.56133 | 1082.04 | 28.07875 | 1082.04 | -70.957 |  | 1082.04 | -31.8048 |
| 1082.09 | 24.45237 | 1082.26 | -28.9482 | 1082.73 | 3.00255 | 1082.73 | 19.50634 | 1082.73 | 24.73967 | 1082.73 | 28.01473 | 1082.73 | -67.5812 |  | 1082.73 | -31.0589 |
| 1082.78 | 24.42699 | 1082.95 | -29.1091 | 1083.42 | 3.34997 | 1083.42 | 19.73205 | 1083.42 | 27.60367 | 1083.42 | 28.03915 | 1083.42 | -64.5198 |  | 1083.42 | -30.5903 |
| 1083.47 | 24.40005 | 1083.64 | -28.7875 | 1084.11 | 3.70445 | 1084.11 | 21.5213 | 1084.11 | 29.67727 | 1084.11 | 29.6271 | 1084.11 | -62.2487 |  | 1084.11 | -30.1146 |
| 1084.16 | 24.37155 | 1084.33 | -28.9286 | 1084.79 | 3.6552 | 1084.79 | 22.22135 | 1084.79 | 31.13354 | 1084.79 | 30.12878 | 1084.79 | -60.5979 |  | 1084.79 | -30.0445 |
| 1084.85 | 24.3417 | 1085.02 | -31.7897 | 1085.48 | 5.24195 | 1085.48 | 24.49336 | 1085.48 | 32.62318 | 1085.48 | 32.1995 | 1085.48 | -58.9107 |  | 1085.48 | -28.3365 |
| 1085.54 | 24.31038 | 1085.71 | -29.8496 | 1086.17 | 7.82753 | 1086.17 | 27.30988 | 1086.17 | 33.19282 | 1086.17 | 34.81473 | 1086.17 | -58.1436 |  | 1086.17 | -25.6298 |
| 1086.23 | 24.27764 | 1086.4 | -31.2763 | 1086.86 | 10.3733 | 1086.86 | 29.21443 | 1086.86 | 34.92305 | 1086.86 | 36.51799 | 1086.86 | -56.2159 |  | 1086.86 | -22.9628 |
| 1086.91 | 24.2432 | 1087.09 | -32.1213 | 1087.55 | 12.2786 | 1087.55 | 30.18881 | 1087.55 | 37.58207 | 1087.55 | 37.29108 | 1087.55 | -53.3595 |  | 1087.55 | -20.9363 |
| 1087.6 | 24.20676 | 1087.78 | -30.5206 | 1088.23 | 10.54232 | 1088.23 | 32.04556 | 1088.23 | 39.64022 | 1088.23 | 38.94946 | 1088.23 | -51.1067 |  | 1088.23 | -22.5532 |
| 1088.29 | 24.16839 | 1088.46 | -32.4614 | 1088.92 | 12.82488 | 1088.92 | 34.03268 | 1088.92 | 40.55081 | 1088.92 | 40.73529 | 1088.92 | -49.9987 |  | 1088.92 | -20.1495 |
| 1088.98 | 24.12758 | 1089.15 | -31.9223 | 1089.61 | 13.80449 | 1089.61 | 34.73628 | 1089.61 | 42.83395 | 1089.61 | 41.23759 | 1089.61 | -47.5181 |  | 1089.61 | -19.0487 |
| 1089.67 | 24.08418 | 1089.84 | -31.3774 | 1090.3 | 14.33018 | 1090.3 | 37.18673 | 1090.3 | 43.73042 | 1090.3 | 43.48675 | 1090.3 | -46.4241 |  | 1090.3 | -18.4018 |
| 1090.36 | 24.03796 | 1090.53 | -32.6259 | 1090.98 | 14.41775 | 1090.98 | 37.27938 | 1090.98 | 44.89089 | 1090.98 | 43.38103 | 1090.98 | -45.0691 |  | 1090.98 | -18.1948 |
| 1091.05 | 23.9889 | 1091.22 | -33.4974 | 1091.67 | 16.1761 | 1091.67 | 37.05377 | 1091.67 | 46.24105 | 1091.67 | 42.95413 | 1091.67 | -43.5214 |  | 1091.67 | -16.3153 |
| 1091.73 | 23.93713 | 1091.91 | -34.2218 | 1092.36 | 17.07438 | 1092.36 | 37.52681 | 1092.36 | 47.92568 | 1092.36 | 43.22588 | 1092.36 | -41.6393 |  | 1092.36 | -15.2958 |
| 1092.42 | 23.88243 | 1092.6 | -33.6778 | 1093.05 | 19.23324 | 1093.05 | 38.11651 | 1093.05 | 49.36188 | 1093.05 | 43.61429 | 1093.05 | -40.0057 |  | 1093.05 | -13.0158 |
| 1093.11 | 23.8243 | 1093.29 | -33.4922 | 1093.73 | 18.25229 | 1093.73 | 38.78644 | 1093.73 | 51.28055 | 1093.73 | 44.08584 | 1093.73 | -37.8924 |  | 1093.73 | -13.8773 |
| 1093.8 | 23.76198 | 1093.98 | -32.7792 | 1094.42 | 18.69245 | 1094.42 | 38.98184 | 1094.42 | 51.70063 | 1094.42 | 44.07995 | 1094.42 | -37.2749 |  | 1094.42 | -13.316 |
| 1094.49 | 23.69501 | 1094.67 | -31.2363 | 1095.11 | 18.79907 | 1095.11 | 39.46176 | 1095.11 | 53.76719 | 1095.11 | 44.35858 | 1095.11 | -35.0108 |  | 1095.11 | -13.0882 |
| 1095.17 | 23.62291 | 1095.36 | -32.2796 | 1095.8 | 21.10013 | 1095.8 | 40.07404 | 1095.8 | 55.47861 | 1095.8 | 44.76957 | 1095.8 | -33.102 |  | 1095.8 | -10.666 |
| 1095.86 | 23.54583 | 1096.04 | -30.8215 | 1096.48 | 22.06823 | 1096.48 | 42.25086 | 1096.48 | 55.3578 | 1096.48 | 46.74802 | 1096.48 | -33.0282 |  | 1096.48 | -9.57842 |
| 1096.55 | 23.46387 | 1096.73 | -31.7257 | 1097.17 | 21.94901 | 1097.17 | 42.77414 | 1097.17 | 55.31095 | 1097.17 | 47.07001 | 1097.17 | -32.8776 |  | 1097.17 | -9.57646 |
| 1097.24 | 23.37667 | 1097.42 | -30.6752 | 1097.86 | 23.42164 | 1097.86 | 42.01349 | 1097.86 | 54.8461 | 1097.86 | 46.10806 | 1097.86 | -33.145 |  | 1097.86 | -7.98266 |
| 1097.93 | 23.28378 | 1098.11 | -28.914 | 1098.54 | 23.53966 | 1098.54 | 42.9717 | 1098.54 | 56.51622 | 1098.54 | 46.86789 | 1098.54 | -31.2802 |  | 1098.54 | -7.74522 |
| 1098.61 | 23.18525 | 1098.8 | -27.4569 | 1099.23 | 23.61103 | 1099.23 | 41.58792 | 1099.23 | 57.22094 | 1099.23 | 45.28283 | 1099.23 | -30.378 |  | 1099.23 | -7.55267 |
| 1099.3 | 23.08055 | 1099.49 | -26.5869 | 1099.92 | 25.16231 | 1099.92 | 42.63808 | 1099.92 | 57.24053 | 1099.92 | 46.13169 | 1099.92 | -30.161 |  | 1099.92 | -5.88021 |
| 1099.99 | 22.96958 | 1100.18 | -25.8572 | 1100.6 | 25.25987 | 1100.6 | 41.18003 | 1100.6 | 57.06984 | 1100.6 | 44.47527 | 1100.6 | -30.1371 |  | 1100.6 | -5.66324 |
| 1100.68 | 22.85204 | 1100.86 | -26.9316 | 1101.29 | 25.19342 | 1101.29 | 42.07021 | 1101.29 | 57.37566 | 1101.29 | 45.16416 | 1101.29 | -29.6338 |  | 1101.29 | -5.6085 |
| 1101.36 | 22.7281 | 1101.55 | -25.6766 | 1101.98 | 24.56522 | 1101.98 | 41.86509 | 1101.98 | 57.38325 | 1101.98 | 44.75775 | 1101.98 | -29.4288 |  | 1101.98 | -6.11553 |
| 1102.05 | 22.5977 | 1102.24 | -25.3775 | 1102.66 | 24.93916 | 1102.66 | 41.8496 | 1102.66 | 58.02369 | 1102.66 | 44.54389 | 1102.66 | -28.5937 |  | 1102.66 | -5.62217 |
| 1102.74 | 22.46078 | 1102.93 | -25.9796 | 1103.35 | 25.49193 | 1103.35 | 43.39959 | 1103.35 | 58.75501 | 1103.35 | 45.89258 | 1103.35 | -27.6649 |  | 1103.35 | -4.94822 |
| 1103.42 | 22.31738 | 1103.62 | -26.3486 | 1104.04 | 25.35129 | 1104.04 | 42.85409 | 1104.04 | 58.34138 | 1104.04 | 45.1458 | 1104.04 | -27.8811 |  | 1104.04 | -4.96768 |
| 1104.11 | 22.16755 | 1104.3 | -26.5047 | 1104.72 | 25.0679 | 1104.72 | 42.52411 | 1104.72 | 57.95925 | 1104.72 | 44.61744 | 1104.72 | -28.0686 |  | 1104.72 | -5.13165 |
| 1104.8 | 22.01129 | 1104.99 | -26.5686 | 1105.41 | 23.86188 | 1105.41 | 44.43511 | 1105.41 | 58.81186 | 1105.41 | 46.32715 | 1105.41 | -27.0186 |  | 1105.41 | -6.21649 |
| 1105.48 | 21.84852 | 1105.68 | -26.9519 | 1106.1 | 25.79536 | 1106.1 | 42.25373 | 1106.1 | 56.54372 | 1106.1 | 43.94448 | 1106.1 | -29.0892 |  | 1106.1 | -4.16184 |
| 1106.17 | 21.67877 | 1106.37 | -26.9095 | 1106.78 | 25.03522 | 1106.78 | 42.60181 | 1106.78 | 56.77253 | 1106.78 | 44.09419 | 1106.78 | -28.6658 |  | 1106.78 | -4.80256 |
| 1106.86 | 21.50235 | 1107.06 | -26.7424 | 1107.47 | 23.13312 | 1107.47 | 42.88026 | 1107.47 | 56.60808 | 1107.47 | 44.17134 | 1107.47 | -28.6328 |  | 1107.47 | -6.58347 |
| 1107.54 | 21.31923 | 1107.74 | -26.8116 | 1108.15 | 25.02918 | 1108.15 | 44.06266 | 1108.15 | 54.72901 | 1108.15 | 45.15537 | 1108.15 | -30.3173 |  | 1108.15 | -4.568 |
| 1108.23 | 21.12958 | 1108.43 | -25.6166 | 1108.84 | 25.50779 | 1108.84 | 43.33093 | 1108.84 | 55.39825 | 1108.84 | 44.22235 | 1108.84 | -29.4506 |  | 1108.84 | -3.96821 |
| 1108.92 | 20.93359 | 1109.12 | -27.5714 | 1109.52 | 26.90149 | 1109.52 | 44.96863 | 1109.52 | 54.18389 | 1109.52 | 45.66168 | 1109.52 | -30.4703 |  | 1109.52 | -2.45509 |
| 1109.6 | 20.73095 | 1109.81 | -29.1027 | 1110.21 | 26.77237 | 1110.21 | 46.5924 | 1110.21 | 53.03682 | 1110.21 | 47.08416 | 1110.21 | -31.4199 |  | 1110.21 | -2.46303 |
| 1110.29 | 20.52195 | 1110.49 | -28.5535 | 1110.9 | 28.19219 | 1110.9 | 45.28423 | 1110.9 | 52.05481 | 1110.9 | 45.57469 | 1110.9 | -32.2045 |  | 1110.9 | -0.92203 |
| 1110.98 | 20.30663 | 1111.18 | -29.5982 | 1111.58 | 29.33032 | 1111.58 | 45.37744 | 1111.58 | 50.89747 | 1111.58 | 45.46953 | 1111.58 | -33.1672 |  | 1111.58 | 0.33552 |
| 1111.66 | 20.08496 | 1111.87 | -30.2028 | 1112.27 | 29.90112 | 1112.27 | 45.0324 | 1112.27 | 50.3688 | 1112.27 | 44.9232 | 1112.27 | -33.4984 |  | 1112.27 | 1.02749 |
| 1112.35 | 19.85736 | 1112.55 | -31.0747 | 1112.95 | 29.20721 | 1112.95 | 45.43445 | 1112.95 | 48.75142 | 1112.95 | 45.12688 | 1112.95 | -34.9212 |  | 1112.95 | 0.453 |
| 1113.04 | 19.62427 | 1113.24 | -34.5167 | 1113.64 | 29.54695 | 1113.64 | 46.03571 | 1113.64 | 45.96878 | 1113.64 | 45.52684 | 1113.64 | -37.5064 |  | 1113.64 | 0.91392 |
| 1113.72 | 19.38609 | 1113.93 | -34.0689 | 1114.32 | 30.33903 | 1114.32 | 45.90287 | 1114.32 | 44.46784 | 1114.32 | 45.19563 | 1114.32 | -38.8127 |  | 1114.32 | 1.82543 |
| 1114.41 | 19.14295 | 1114.61 | -35.3268 | 1115.01 | 29.39936 | 1115.01 | 45.79667 | 1115.01 | 43.42285 | 1115.01 | 44.88814 | 1115.01 | -39.6603 |  | 1115.01 | 1.00693 |
| 1115.09 | 18.89548 | 1115.3 | -35.2508 | 1115.69 | 29.57646 | 1115.69 | 45.86052 | 1115.69 | 42.77364 | 1115.69 | 44.75361 | 1115.69 | -40.1149 |  | 1115.69 | 1.30345 |
| 1115.78 | 18.64402 | 1115.99 | -36.6395 | 1116.38 | 30.07788 | 1116.38 | 44.92199 | 1116.38 | 39.82528 | 1116.38 | 43.61379 | 1116.38 | -42.8658 |  | 1116.38 | 1.92606 |
| 1116.47 | 18.38876 | 1116.67 | -35.9323 | 1117.06 | 31.86048 | 1117.06 | 43.6774 | 1117.06 | 38.49842 | 1117.06 | 42.17083 | 1117.06 | -43.998 |  | 1117.06 | 3.82807 |
| 1117.15 | 18.12993 | 1117.36 | -35.1905 | 1117.75 | 31.84927 | 1117.75 | 44.32634 | 1117.75 | 37.27748 | 1117.75 | 42.61848 | 1117.75 | -45.0215 |  | 1117.75 | 3.93804 |
| 1117.84 | 17.86785 | 1118.05 | -33.0491 | 1118.43 | 31.8057 | 1118.43 | 43.97961 | 1118.43 | 36.61705 | 1118.43 | 42.07338 | 1118.43 | -45.4873 |  | 1118.43 | 4.01389 |
| 1118.52 | 17.6029 | 1118.73 | -31.7105 | 1119.12 | 31.33724 | 1119.12 | 42.28698 | 1119.12 | 36.03454 | 1119.12 | 40.17945 | 1119.12 | -45.8724 |  | 1119.12 | 3.66661 |
| 1119.21 | 17.33523 | 1119.42 | -29.9416 | 1119.8 | 30.97399 | 1119.8 | 40.19458 | 1119.8 | 36.08701 | 1119.8 | 37.88868 | 1119.8 | -45.6253 |  | 1119.8 | 3.42278 |
| 1119.89 | 17.06531 | 1120.11 | -30.6618 | 1120.49 | 30.70937 | 1120.49 | 38.37804 | 1120.49 | 34.84349 | 1120.49 | 35.87085 | 1120.49 | -46.6714 |  | 1120.49 | 3.27933 |
| 1120.58 | 16.79369 | 1120.79 | -27.1783 | 1121.17 | 29.54336 | 1121.17 | 36.13878 | 1121.17 | 34.84322 | 1121.17 | 33.43322 | 1121.17 | -46.477 |  | 1121.17 | 2.23275 |
| 1121.26 | 16.52085 | 1121.48 | -28.4706 | 1121.86 | 28.51415 | 1121.86 | 34.87795 | 1121.86 | 33.00691 | 1121.86 | 31.97109 | 1121.86 | -48.1159 |  | 1121.86 | 1.32472 |
| 1121.95 | 16.24736 | 1122.17 | -26.7054 | 1122.54 | 28.50846 | 1122.54 | 35.12949 | 1122.54 | 30.64112 | 1122.54 | 32.02426 | 1122.54 | -50.2871 |  | 1122.54 | 1.43845 |
| 1122.63 | 15.97363 | 1122.85 | -27.3346 | 1123.23 | 30.93153 | 1123.23 | 34.0671 | 1123.23 | 27.86399 | 1123.23 | 30.76058 | 1123.23 | -52.8667 |  | 1123.23 | 3.98269 |
| 1123.32 | 15.69986 | 1123.54 | -28.4336 | 1123.91 | 31.21399 | 1123.91 | 33.67317 | 1123.91 | 27.69541 | 1123.91 | 30.16828 | 1123.91 | -52.8407 |  | 1123.91 | 4.38458 |
| 1124 | 15.42624 | 1124.22 | -27.4006 | 1124.6 | 31.92862 | 1124.6 | 32.02078 | 1124.6 | 26.92985 | 1124.6 | 28.3146 | 1124.6 | -53.4088 |  | 1124.6 | 5.22039 |
| 1124.69 | 15.15311 | 1124.91 | -28.2453 | 1125.28 | 31.94571 | 1125.28 | 30.8104 | 1125.28 | 25.65378 | 1125.28 | 26.90584 | 1125.28 | -54.4903 |  | 1125.28 | 5.3569 |
| 1125.37 | 14.8807 | 1125.6 | -29.7952 | 1125.96 | 32.33398 | 1125.96 | 30.38178 | 1125.96 | 22.99027 | 1125.96 | 26.27884 | 1125.96 | -56.9592 |  | 1125.96 | 5.86458 |
| 1126.06 | 14.60927 | 1126.28 | -30.1527 | 1126.65 | 32.45088 | 1126.65 | 30.41215 | 1126.65 | 21.85271 | 1126.65 | 26.10793 | 1126.65 | -57.8993 |  | 1126.65 | 6.10266 |
| 1126.74 | 14.33925 | 1126.97 | -31.8808 | 1127.33 | 32.75503 | 1127.33 | 30.06412 | 1127.33 | 20.97116 | 1127.33 | 25.56152 | 1127.33 | -58.5863 |  | 1127.33 | 6.52623 |
| 1127.43 | 14.0712 | 1127.65 | -32.4003 | 1128.01 | 32.16753 | 1128.01 | 30.25061 | 1128.01 | 20.15721 | 1128.01 | 25.54964 | 1128.01 | -59.2056 |  | 1128.01 | 6.05816 |
| 1128.11 | 13.8054 | 1128.34 | -33.6148 | 1128.7 | 33.29839 | 1128.7 | 28.71592 | 1128.7 | 19.36448 | 1128.7 | 23.81366 | 1128.7 | -59.8009 |  | 1128.7 | 7.31019 |
| 1128.8 | 13.54202 | 1129.02 | -34.9745 | 1129.38 | 33.19795 | 1129.38 | 28.32496 | 1129.38 | 19.50799 | 1129.38 | 23.22432 | 1129.38 | -59.4628 |  | 1129.38 | 7.32917 |
| 1129.48 | 13.28092 | 1129.71 | -35.7112 | 1130.07 | 34.03096 | 1130.07 | 27.10478 | 1130.07 | 17.11428 | 1130.07 | 21.80285 | 1130.07 | -61.659 |  | 1130.07 | 8.28336 |
| 1130.17 | 13.02208 | 1130.39 | -35.2814 | 1130.75 | 34.06652 | 1130.75 | 26.86227 | 1130.75 | 15.82363 | 1130.75 | 21.36197 | 1130.75 | -62.755 |  | 1130.75 | 8.43834 |
| 1130.85 | 12.76552 | 1131.08 | -34.3069 | 1131.43 | 34.69709 | 1131.43 | 24.59075 | 1131.43 | 13.91275 | 1131.43 | 18.89208 | 1131.43 | -64.4713 |  | 1131.43 | 9.18834 |
| 1131.53 | 12.5117 | 1131.76 | -36.1802 | 1132.12 | 36.59199 | 1132.12 | 25.56608 | 1132.12 | 12.35862 | 1132.12 | 19.66611 | 1132.12 | -65.828 |  | 1132.12 | 11.20441 |
| 1132.22 | 12.26085 | 1132.45 | -35.8815 | 1132.8 | 36.0515 | 1132.8 | 25.33203 | 1132.8 | 11.94103 | 1132.8 | 19.23369 | 1132.8 | -66.051 |  | 1132.8 | 10.78334 |
| 1132.9 | 12.01302 | 1133.13 | -35.6941 | 1133.48 | 36.23521 | 1133.48 | 23.98268 | 1133.48 | 11.1778 | 1133.48 | 17.68596 | 1133.48 | -66.6196 |  | 1133.48 | 11.08647 |
| 1133.59 | 11.76822 | 1133.82 | -37.0344 | 1134.17 | 36.13845 | 1134.17 | 24.57547 | 1134.17 | 9.85206 | 1134.17 | 18.07746 | 1134.17 | -67.7479 |  | 1134.17 | 11.1109 |
| 1134.27 | 11.52661 | 1134.5 | -36.8456 | 1134.85 | 33.81365 | 1134.85 | 22.92221 | 1134.85 | 8.64055 | 1134.85 | 16.22583 | 1134.85 | -68.7648 |  | 1134.85 | 8.90552 |
| 1134.95 | 11.28812 | 1135.19 | -37.267 | 1135.53 | 31.6121 | 1135.53 | 22.77857 | 1135.53 | 6.35175 | 1135.53 | 15.88382 | 1135.53 | -70.859 |  | 1135.53 | 6.82339 |
| 1135.64 | 11.05289 | 1135.87 | -38.7464 | 1136.22 | 31.8139 | 1136.22 | 21.39255 | 1136.22 | 3.37676 | 1136.22 | 14.29651 | 1136.22 | -73.6365 |  | 1136.22 | 7.14636 |
| 1136.32 | 10.82074 | 1136.56 | -36.9963 | 1136.9 | 31.30246 | 1136.9 | 20.02893 | 1136.9 | 2.20362 | 1136.9 | 12.73452 | 1136.9 | -74.6151 |  | 1136.9 | 6.75435 |
| 1137.01 | 10.59171 | 1137.24 | -38.6336 | 1137.58 | 31.13672 | 1137.58 | 18.43786 | 1137.58 | 1.05596 | 1137.58 | 10.94507 | 1137.58 | -75.5681 |  | 1137.58 | 6.70802 |
| 1137.69 | 10.36582 | 1137.93 | -39.8527 | 1138.27 | 30.39274 | 1138.27 | 16.34421 | 1138.27 | -0.59946 | 1138.27 | 8.65013 | 1138.27 | -77.0261 |  | 1138.27 | 6.08522 |
| 1138.37 | 10.14302 | 1138.61 | -40.3007 | 1138.95 | 30.19895 | 1138.95 | 16.0551 | 1138.95 | -1.35006 | 1138.95 | 8.16265 | 1138.95 | -77.5821 |  | 1138.95 | 6.01086 |
| 1139.06 | 9.92324 | 1139.3 | -39.1688 | 1139.63 | 30.03626 | 1139.63 | 14.6464 | 1139.63 | -1.14736 | 1139.63 | 6.55557 | 1139.63 | -77.1848 |  | 1139.63 | 5.96759 |
| 1139.74 | 9.70563 | 1139.98 | -38.1713 | 1140.31 | 30.80906 | 1140.31 | 11.22083 | 1140.31 | -2.42917 | 1140.31 | 2.93163 | 1140.31 | -78.272 |  | 1140.31 | 6.85981 |
| 1140.42 | 9.49021 | 1140.67 | -38.1553 | 1141 | 28.7463 | 1141 | 11.72899 | 1141 | -1.75173 | 1141 | 3.23849 | 1141 | -77.3971 |  | 1141 | 4.91822 |
| 1141.11 | 9.2771 | 1141.35 | -37.2588 | 1141.68 | 28.69196 | 1141.68 | 12.06265 | 1141.68 | -1.48495 | 1141.68 | 3.37379 | 1141.68 | -76.9357 |  | 1141.68 | 4.9833 |
| 1141.79 | 9.06614 | 1142.03 | -38.2076 | 1142.36 | 29.52342 | 1142.36 | 12.50771 | 1142.36 | -1.8135 | 1142.36 | 3.62047 | 1142.36 | -77.0697 |  | 1142.36 | 5.93418 |
| 1142.47 | 8.85742 | 1142.72 | -37.835 | 1143.04 | 27.31547 | 1143.04 | 11.33766 | 1143.04 | 0.32384 | 1143.04 | 2.25205 | 1143.04 | -74.7377 |  | 1143.04 | 3.84566 |
| 1143.16 | 8.65081 | 1143.4 | -37.0185 | 1143.73 | 25.3938 | 1143.73 | 9.60956 | 1143.73 | -0.59224 | 1143.73 | 0.32265 | 1143.73 | -75.3248 |  | 1143.73 | 2.04516 |
| 1143.84 | 8.44603 | 1144.09 | -37.9241 | 1144.41 | 25.65224 | 1144.41 | 8.66718 | 1144.41 | -0.89 | 1144.41 | -0.8181 | 1144.41 | -75.2072 |  | 1144.41 | 2.42303 |
| 1144.52 | 8.24282 | 1144.77 | -36.9084 | 1145.09 | 25.92539 | 1145.09 | 5.95303 | 1145.09 | -1.19599 | 1145.09 | -3.73062 | 1145.09 | -75.0979 |  | 1145.09 | 2.81559 |
| 1145.21 | 8.04063 | 1145.45 | -35.4543 | 1145.77 | 25.21735 | 1145.77 | 4.49477 | 1145.77 | -2.39884 | 1145.77 | -5.38725 | 1145.77 | -75.8854 |  | 1145.77 | 2.22698 |
| 1145.89 | 7.83952 | 1146.14 | -36.477 | 1146.46 | 24.63768 | 1146.46 | 3.61866 | 1146.46 | -3.46588 | 1146.46 | -6.46466 | 1146.46 | -76.531 |  | 1146.46 | 1.76849 |
| 1146.57 | 7.63935 | 1146.82 | -38.2999 | 1147.14 | 24.39691 | 1147.14 | 4.17079 | 1147.14 | -4.93834 | 1147.14 | -6.1109 | 1147.14 | -77.5881 |  | 1147.14 | 1.64713 |
| 1147.25 | 7.4398 | 1147.51 | -39.9628 | 1147.82 | 25.28272 | 1147.82 | 3.13019 | 1147.82 | -4.7077 | 1147.82 | -7.34987 | 1147.82 | -76.9421 |  | 1147.82 | 2.65236 |
| 1147.94 | 7.24041 | 1148.19 | -40.5205 | 1148.5 | 24.87225 | 1148.5 | 3.91077 | 1148.5 | -4.53176 | 1148.5 | -6.76767 | 1148.5 | -76.3509 |  | 1148.5 | 2.36132 |
| 1148.62 | 7.04107 | 1148.87 | -42.1548 | 1149.18 | 23.41296 | 1149.18 | 4.17802 | 1149.18 | -3.79092 | 1149.18 | -6.6988 | 1149.18 | -75.1947 |  | 1149.18 | 1.02145 |
| 1149.3 | 6.84165 | 1149.56 | -41.4098 | 1149.86 | 23.10457 | 1149.86 | 5.24292 | 1149.86 | -3.02326 | 1149.86 | -5.83226 | 1149.86 | -74.0117 |  | 1149.86 | 0.83248 |
| 1149.98 | 6.642 | 1150.24 | -39.6694 | 1150.55 | 22.53756 | 1150.55 | 5.9608 | 1150.55 | -4.1916 | 1150.55 | -5.31567 | 1150.55 | -74.7586 |  | 1150.55 | 0.38665 |
| 1150.67 | 6.44198 | 1150.92 | -38.9806 | 1151.23 | 22.84298 | 1151.23 | 6.09731 | 1151.23 | -3.04791 | 1151.23 | -5.37754 | 1151.23 | -73.1996 |  | 1151.23 | 0.81149 |
| 1151.35 | 6.24138 | 1151.61 | -39.0754 | 1151.91 | 22.194 | 1151.91 | 5.85776 | 1151.91 | -1.85152 | 1151.91 | -5.81546 | 1151.91 | -71.5878 |  | 1151.91 | 0.28193 |
| 1152.03 | 6.0402 | 1152.29 | -38.2906 | 1152.59 | 21.38835 | 1152.59 | 4.07331 | 1152.59 | -1.88199 | 1152.59 | -7.79829 | 1152.59 | -71.203 |  | 1152.59 | -0.40429 |
| 1152.71 | 5.83844 | 1152.97 | -38.1165 | 1153.27 | 21.47173 | 1153.27 | 4.17592 | 1153.27 | -3.12402 | 1153.27 | -7.89405 | 1153.27 | -72.0297 |  | 1153.27 | -0.2015 |
| 1153.4 | 5.63603 | 1153.65 | -36.8727 | 1153.95 | 21.45247 | 1153.95 | 4.06972 | 1153.95 | -3.60335 | 1153.95 | -8.19863 | 1153.95 | -72.0937 |  | 1153.95 | -0.10133 |
| 1154.08 | 5.43287 | 1154.34 | -35.1687 | 1154.63 | 21.27996 | 1154.63 | 4.75272 | 1154.63 | -5.50872 | 1154.63 | -7.714 | 1154.63 | -73.5837 |  | 1154.63 | -0.15442 |
| 1154.76 | 5.22883 | 1155.02 | -35.4501 | 1155.32 | 19.75962 | 1155.32 | 3.72726 | 1155.32 | -5.64157 | 1155.32 | -8.94075 | 1155.32 | -73.2951 |  | 1155.32 | -1.55359 |
| 1155.44 | 5.02369 | 1155.7 | -35.5277 | 1156 | 19.65409 | 1156 | 4.11498 | 1156 | -7.11835 | 1156 | -8.7514 | 1156 | -74.3565 |  | 1156 | -1.5397 |
| 1156.12 | 4.81723 | 1156.39 | -32.7416 | 1156.68 | 17.98856 | 1156.68 | 3.5878 | 1156.68 | -5.28277 | 1156.68 | -9.47695 | 1156.68 | -72.1056 |  | 1156.68 | -3.0858 |
| 1156.81 | 4.60942 | 1157.07 | -31.4294 | 1157.36 | 16.23048 | 1157.36 | 4.67219 | 1157.36 | -6.95347 | 1157.36 | -8.59094 | 1157.36 | -73.361 |  | 1157.36 | -4.72446 |
| 1157.49 | 4.40014 | 1157.75 | -32.9299 | 1158.04 | 15.33319 | 1158.04 | 3.08383 | 1158.04 | -7.32319 | 1158.04 | -10.3777 | 1158.04 | -73.3154 |  | 1158.04 | -5.50234 |
| 1158.17 | 4.1895 | 1158.43 | -33.5934 | 1158.72 | 13.37738 | 1158.72 | 1.16412 | 1158.72 | -8.44687 | 1158.72 | -12.4958 | 1158.72 | -74.0237 |  | 1158.72 | -7.33872 |
| 1158.85 | 3.97723 | 1159.12 | -33.897 | 1159.4 | 11.4353 | 1159.4 | 1.86362 | 1159.4 | -9.30035 | 1159.4 | -11.9946 | 1159.4 | -74.4619 |  | 1159.4 | -9.16138 |
| 1159.53 | 3.76318 | 1159.8 | -33.9246 | 1160.08 | 10.73831 | 1160.08 | 2.2496 | 1160.08 | -9.2103 | 1160.08 | -11.807 | 1160.08 | -73.9565 |  | 1160.08 | -9.73894 |
| 1160.21 | 3.54755 | 1160.48 | -34.5231 | 1160.76 | 8.61004 | 1160.76 | 0.39124 | 1160.76 | -9.09316 | 1160.76 | -13.8638 | 1160.76 | -73.424 |  | 1160.76 | -11.7478 |
| 1160.89 | 3.33049 | 1161.16 | -34.8716 | 1161.44 | 6.27933 | 1161.44 | 1.04525 | 1161.44 | -9.5086 | 1161.44 | -13.4081 | 1161.44 | -73.4241 |  | 1161.44 | -13.9591 |
| 1161.58 | 3.11211 | 1161.84 | -35.7352 | 1162.12 | 5.19823 | 1162.12 | 0.74475 | 1162.12 | -9.8962 | 1162.12 | -13.907 | 1162.12 | -73.3964 |  | 1162.12 | -14.9208 |
| 1162.26 | 2.89275 | 1162.53 | -35.1326 | 1162.8 | 3.41203 | 1162.8 | 0.03818 | 1162.8 | -9.30007 | 1162.8 | -14.8119 | 1162.8 | -72.3849 |  | 1162.8 | -16.5875 |
| 1162.94 | 2.67272 | 1163.21 | -34.0086 | 1163.48 | 2.42701 | 1163.48 | -0.43887 | 1163.48 | -8.57218 | 1163.48 | -15.0651 | 1163.48 | -71.2417 |  | 1163.48 | -17.4532 |
| 1163.62 | 2.45206 | 1163.89 | -36.0311 | 1164.17 | 1.34485 | 1164.17 | -0.97249 | 1164.17 | -8.10808 | 1164.17 | -14.3881 | 1164.17 | -70.3561 |  | 1164.17 | -18.4141 |
| 1164.3 | 2.23095 | 1164.57 | -38.487 | 1164.85 | 0.16151 | 1164.85 | -1.60287 | 1164.85 | -9.44513 | 1164.85 | -13.8254 | 1164.85 | -71.2778 |  | 1164.85 | -19.478 |
| 1164.98 | 2.00963 | 1165.25 | -38.3076 | 1165.53 | -0.65143 | 1165.53 | -3.42993 | 1165.53 | -7.96453 | 1165.53 | -14.4593 | 1165.53 | -69.3819 |  | 1165.53 | -20.1716 |
| 1165.66 | 1.78816 | 1165.94 | -38.5236 | 1166.21 | -1.01281 | 1166.21 | -3.04934 | 1166.21 | -6.41236 | 1166.21 | -12.8856 | 1166.21 | -67.4144 |  | 1166.21 | -20.4135 |
| 1166.34 | 1.56664 | 1166.62 | -38.3645 | 1166.89 | -2.70889 | 1166.89 | -5.38031 | 1166.89 | -5.11291 | 1166.89 | -14.0235 | 1166.89 | -65.6996 |  | 1166.89 | -21.9902 |
| 1167.02 | 1.34546 | 1167.3 | -39.4065 | 1167.06 | -3.03365 | 1167.06 | -4.09568 | 1167.06 | -4.18959 | 1167.06 | -12.4406 | 1167.06 | -64.6724 |  | 1167.06 | -22.2851 |
| 1167.7 | 1.12471 | 1167.98 | -39.8153 | 1167.75 | -3.33588 | 1167.75 | -5.47379 | 1167.75 | -5.15486 | 1167.75 | -12.6081 | 1167.75 | -65.2163 |  | 1167.75 | -22.4661 |
| 1168.38 | 0.90466 | 1168.66 | -41.4254 | 1168.43 | -3.86283 | 1168.43 | -5.40377 | 1168.43 | -4.25774 | 1168.43 | -11.345 | 1168.43 | -63.9038 |  | 1168.43 | -22.8737 |
| 1169.06 | 0.68556 | 1169.35 | -41.4612 | 1169.11 | -2.50351 | 1169.11 | -3.33982 | 1169.11 | -4.76921 | 1169.11 | -8.08791 | 1169.11 | -64 |  | 1169.11 | -21.3949 |
| 1169.75 | 0.46784 | 1170.03 | -42.4069 | 1169.79 | -1.3834 | 1169.79 | -2.64804 | 1169.79 | -3.09263 | 1169.79 | -6.20302 | 1169.79 | -61.908 |  | 1169.79 | -20.1554 |
| 1170.43 | 0.25177 | 1170.71 | -44.3921 | 1170.47 | -0.04329 | 1170.47 | -2.94351 | 1170.47 | -1.82268 | 1170.47 | -5.30539 | 1170.47 | -60.2228 |  | 1170.47 | -18.6959 |
| 1171.11 | 0.03758 | 1171.39 | -44.0377 | 1171.16 | -0.33513 | 1171.16 | -3.77417 | 1171.16 | 0 | 1171.16 | -4.9254 | 1171.16 | -57.9786 |  | 1171.16 | -18.8665 |
| 1171.79 | -0.17451 | 1172.07 | -43.648 | 1171.84 | -0.49933 | 1171.84 | -2.48415 | 1171.84 | 0.85514 | 1171.84 | -2.44228 | 1171.84 | -57.4178 |  | 1171.84 | -18.9113 |
| 1172.47 | -0.38421 | 1172.75 | -43.525 | 1172.52 | -0.04891 | 1172.52 | -1.22607 | 1172.52 | 1.4589 | 1172.52 | 0.0089 | 1172.52 | -57.1084 |  | 1172.52 | -18.3415 |
| 1173.15 | -0.59129 | 1173.43 | -44.6088 | 1173.2 | -0.95908 | 1173.2 | -0.06172 | 1173.2 | 1.85582 | 1173.2 | 2.36635 | 1173.2 | -57.0058 |  | 1173.2 | -19.1322 |
| 1173.83 | -0.79518 | 1174.11 | -43.9203 | 1173.88 | -0.03297 | 1173.88 | 0.12459 | 1173.88 | 2.50335 | 1173.88 | 3.74576 | 1173.88 | -56.6526 |  | 1173.88 | -18.0867 |
| 1174.51 | -0.99584 | 1174.79 | -43.7198 | 1174.56 | 0 | 1174.56 | 0.56208 | 1174.56 | 3.23052 | 1174.56 | 5.37635 | 1174.56 | -56.2197 |  | 1174.56 | -17.9343 |
| 1175.19 | -1.1931 | 1175.48 | -44.075 | 1175.24 | -0.21569 | 1175.24 | 0.70604 | 1175.24 | 4.35535 | 1175.24 | 6.71341 | 1175.24 | -55.3892 |  | 1175.24 | -18.0093 |
| 1175.87 | -1.38699 | 1176.16 | -42.7268 | 1175.92 | -0.35683 | 1175.92 | 0 | 1175.92 | 6.84256 | 1175.92 | 7.20047 | 1175.92 | -53.1964 |  | 1175.92 | -18.0098 |
| 1176.55 | -1.5772 | 1176.84 | -43.1562 | 1176.6 | -1.46303 | 1176.6 | 0.47965 | 1176.6 | 7.50959 | 1176.6 | 7.73989 | 1176.6 | -52.8236 |  | 1176.6 | -18.9753 |
| 1177.23 | -1.76337 | 1177.52 | -42.1569 | 1177.29 | -0.72065 | 1177.29 | 1.70372 | 1177.29 | 7.55549 | 1177.29 | 9.02459 | 1177.29 | -53.0764 |  | 1177.29 | -18.0902 |
| 1177.9 | -1.94498 | 1178.2 | -42.0456 | 1177.97 | 0.49011 | 1177.97 | 3.99867 | 1177.97 | 5.78375 | 1177.97 | 11.3793 | 1177.97 | -55.1425 |  | 1177.97 | -16.7387 |
| 1178.58 | -2.1216 | 1178.88 | -43.6607 | 1178.65 | 0.53679 | 1178.65 | 5.4395 | 1178.65 | 5.124 | 1178.65 | 12.87989 | 1178.65 | -56.0966 |  | 1178.65 | -16.5514 |
| 1179.27 | -2.293 | 1179.56 | -42.776 | 1179.33 | -0.22942 | 1179.33 | 9.11268 | 1179.33 | 6.08172 | 1179.33 | 16.61283 | 1179.33 | -55.4332 |  | 1179.33 | -17.1769 |
| 1179.94 | -2.45889 | 1180.24 | -42.4208 | 1180.01 | -1.1107 | 1180.01 | 10.75882 | 1180.01 | 7.8317 | 1180.01 | 18.31873 | 1180.01 | -53.9775 |  | 1180.01 | -17.9175 |
| 1180.62 | -2.61922 | 1180.92 | -40.7549 | 1180.69 | -1.57017 | 1180.69 | 12.06398 | 1180.69 | 10.26505 | 1180.69 | 19.68365 | 1180.69 | -51.8385 |  | 1180.69 | -18.2363 |
| 1181.3 | -2.7733 | 1181.6 | -43.242 | 1181.37 | -1.54184 | 1181.37 | 12.82464 | 1181.37 | 12.63917 | 1181.37 | 20.50408 | 1181.37 | -49.7587 |  | 1181.37 | -18.0673 |
| 1181.98 | -2.92065 | 1182.28 | -43.4274 | 1182.05 | -2.58404 | 1182.05 | 13.05152 | 1182.05 | 13.33194 | 1182.05 | 20.79072 | 1182.05 | -49.3603 |  | 1182.05 | -18.9688 |
| 1182.66 | -3.06175 | 1182.96 | -41.9636 | 1182.73 | -2.40366 | 1182.73 | 12.13715 | 1182.73 | 15.33473 | 1182.73 | 19.93611 | 1182.73 | -47.6518 |  | 1182.73 | -18.6477 |
| 1183.34 | -3.19629 | 1183.64 | -42.022 | 1183.41 | -1.31264 | 1183.41 | 13.95998 | 1183.41 | 17.5948 | 1183.41 | 21.8187 | 1183.41 | -45.686 |  | 1183.41 | -17.416 |
| 1184.02 | -3.32411 | 1184.32 | -40.4337 | 1184.09 | 0.13077 | 1184.09 | 13.05117 | 1184.09 | 19.61372 | 1184.09 | 20.96965 | 1184.09 | -43.9615 |  | 1184.09 | -15.832 |
| 1184.7 | -3.44508 | 1185 | -41.0791 | 1184.77 | 0.01894 | 1184.77 | 13.82695 | 1184.77 | 21.90334 | 1184.77 | 21.80519 | 1184.77 | -41.9662 |  | 1184.77 | -15.8031 |
| 1185.38 | -3.56048 | 1185.68 | -40.4579 | 1185.45 | -0.44177 | 1185.45 | 14.70633 | 1185.45 | 24.24441 | 1185.45 | 22.74433 | 1185.45 | -39.9194 |  | 1185.45 | -16.1231 |
| 1186.06 | -3.67048 | 1186.36 | -37.6227 | 1186.13 | -0.79204 | 1186.13 | 18.15506 | 1186.13 | 24.78158 | 1186.13 | 26.25282 | 1186.13 | -39.6766 |  | 1186.13 | -16.3327 |
| 1186.73 | -3.77532 | 1187.04 | -38.1758 | 1186.81 | 1.01969 | 1186.81 | 17.92196 | 1186.81 | 24.83426 | 1186.81 | 26.07948 | 1186.81 | -39.9182 |  | 1186.81 | -14.3803 |
| 1187.41 | -3.87669 | 1187.72 | -37.9428 | 1187.49 | 0.20108 | 1187.49 | 18.50879 | 1187.49 | 25.50521 | 1187.49 | 26.72608 | 1187.49 | -39.5416 |  | 1187.49 | -15.0583 |
| 1188.09 | -3.97458 | 1188.4 | -39.408 | 1188.17 | 1.59564 | 1188.17 | 19.1589 | 1188.17 | 27.64696 | 1188.17 | 27.43594 | 1188.17 | -37.6942 |  | 1188.17 | -13.523 |
| 1188.77 | -4.06889 | 1189.08 | -38.9031 | 1188.85 | 1.42429 | 1188.85 | 20.03699 | 1188.85 | 29.04125 | 1188.85 | 28.3738 | 1188.85 | -36.5942 |  | 1188.85 | -13.5537 |
| 1189.45 | -4.15958 | 1189.76 | -39.7223 | 1189.53 | 1.57865 | 1189.53 | 21.37906 | 1189.53 | 28.08329 | 1189.53 | 29.77563 | 1189.53 | -37.8465 |  | 1189.53 | -13.2586 |
| 1190.13 | -4.2464 | 1190.44 | -40.5053 | 1190.21 | 1.22384 | 1190.21 | 21.53323 | 1190.21 | 28.94635 | 1190.21 | 29.98955 | 1190.21 | -37.2778 |  | 1190.21 | -13.4728 |
| 1190.81 | -4.3296 | 1191.12 | -40.7927 | 1190.89 | 1.60966 | 1190.89 | 21.84654 | 1190.89 | 28.04491 | 1190.89 | 30.36263 | 1190.89 | -38.4735 |  | 1190.89 | -12.9463 |
| 1191.48 | -4.40947 | 1191.79 | -42.7876 | 1191.57 | 1.41926 | 1191.57 | 20.71077 | 1191.57 | 29.35723 | 1191.57 | 29.28662 | 1191.57 | -37.4555 |  | 1191.57 | -12.996 |
| 1192.16 | -4.48631 | 1192.47 | -43.2808 | 1192.25 | 2.98809 | 1192.25 | 22.34761 | 1192.25 | 30.64181 | 1192.25 | 30.98322 | 1192.25 | -36.4653 |  | 1192.25 | -11.2865 |
| 1192.84 | -4.5604 | 1193.15 | -44.0593 | 1192.93 | 4.81266 | 1192.93 | 25.13144 | 1192.93 | 31.99525 | 1192.93 | 33.82681 | 1192.93 | -35.4062 |  | 1192.93 | -9.32124 |
| 1193.52 | -4.63182 | 1193.83 | -45.454 | 1193.61 | 3.7659 | 1193.61 | 25.54873 | 1193.61 | 33.06458 | 1193.61 | 34.30386 | 1193.61 | -34.6312 |  | 1193.61 | -10.2273 |
| 1194.2 | -4.70093 | 1194.51 | -44.93 | 1194.29 | 2.62643 | 1194.29 | 28.04949 | 1194.29 | 33.95689 | 1194.29 | 36.86438 | 1194.29 | -34.0332 |  | 1194.29 | -11.2261 |
| 1194.87 | -4.7682 | 1195.19 | -45.6282 | 1194.97 | 4.48713 | 1194.97 | 31.1751 | 1194.97 | 34.82702 | 1194.97 | 40.04975 | 1194.97 | -33.4574 |  | 1194.97 | -9.22473 |
| 1195.55 | -4.83372 | 1195.87 | -46.0618 | 1195.65 | 6.53021 | 1195.65 | 31.09234 | 1195.65 | 34.02727 | 1195.65 | 40.02675 | 1195.65 | -34.5515 |  | 1195.65 | -7.04097 |
| 1196.23 | -4.89754 | 1196.55 | -44.2706 | 1196.33 | 8.1449 | 1196.33 | 31.05422 | 1196.33 | 34.04891 | 1196.33 | 40.04839 | 1196.33 | -34.8241 |  | 1196.33 | -5.28561 |
| 1196.91 | -4.95978 | 1197.23 | -43.623 | 1197 | 8.00268 | 1197 | 30.29554 | 1197 | 32.77056 | 1197 | 39.34859 | 1197 | -36.3925 |  | 1197 | -5.28921 |
| 1197.58 | -5.02039 | 1197.9 | -44.1816 | 1197.68 | 9.54058 | 1197.68 | 32.06839 | 1197.68 | 31.28862 | 1197.68 | 41.1812 | 1197.68 | -38.1688 |  | 1197.68 | -3.61063 |
| 1198.26 | -5.07936 | 1198.58 | -45.2266 | 1198.36 | 9.25127 | 1198.36 | 30.77431 | 1198.36 | 30.51218 | 1198.36 | 39.94689 | 1198.36 | -39.2395 |  | 1198.36 | -3.75927 |
| 1198.94 | -5.13717 | 1199.26 | -43.5918 | 1199.04 | 8.25789 | 1199.04 | 31.11017 | 1199.04 | 30.61225 | 1199.04 | 40.34251 | 1199.04 | -39.4338 |  | 1199.04 | -4.61197 |
| 1199.62 | -5.19374 | 1199.94 | -43.8413 | 1199.72 | 7.62416 | 1199.72 | 32.62734 | 1199.72 | 30.60096 | 1199.72 | 41.91943 | 1199.72 | -39.7394 |  | 1199.72 | -5.10502 |
| 1200.3 | -5.2489 | 1200.62 | -42.8156 | 1200.4 | 6.91202 | 1200.4 | 30.81534 | 1200.4 | 30.79841 | 1200.4 | 40.1672 | 1200.4 | -39.8363 |  | 1200.4 | -5.67648 |
| 1200.97 | -5.30274 | 1201.3 | -43.0303 | 1201.08 | 7.29189 | 1201.08 | 31.74113 | 1201.08 | 31.30567 | 1201.08 | 41.15274 | 1201.08 | -39.6233 |  | 1201.08 | -5.15593 |
| 1201.65 | -5.3557 | 1201.97 | -43.6836 | 1201.76 | 6.36612 | 1201.76 | 32.01881 | 1201.76 | 29.39293 | 1201.76 | 41.49019 | 1201.76 | -41.8304 |  | 1201.76 | -5.94103 |
| 1202.33 | -5.40802 | 1202.65 | -43.6804 | 1202.43 | 6.78695 | 1202.43 | 31.90703 | 1202.43 | 30.97752 | 1202.43 | 41.43729 | 1202.43 | -40.5358 |  | 1202.43 | -5.38159 |
| 1203 | -5.46012 | 1203.33 | -42.6059 | 1203.11 | 7.58321 | 1203.11 | 30.26941 | 1203.11 | 29.95565 | 1203.11 | 39.85943 | 1203.11 | -41.852 |  | 1203.11 | -4.44465 |
| 1203.68 | -5.5121 | 1204.01 | -42.9708 | 1203.79 | 7.0754 | 1203.79 | 28.30388 | 1203.79 | 30.19633 | 1203.79 | 37.95366 | 1203.79 | -41.9057 |  | 1203.79 | -4.81178 |
| 1204.36 | -5.56437 | 1204.69 | -42.8627 | 1204.47 | 8.3631 | 1204.47 | 27.15978 | 1204.47 | 31.24357 | 1204.47 | 36.86932 | 1204.47 | -41.1527 |  | 1204.47 | -3.3834 |
| 1205.04 | -5.61681 | 1205.36 | -42.6579 | 1205.15 | 7.43379 | 1205.15 | 27.52993 | 1205.15 | 32.72768 | 1205.15 | 37.29923 | 1205.15 | -39.963 |  | 1205.15 | -4.17203 |
| 1205.71 | -5.66974 | 1206.04 | -41.7312 | 1205.83 | 8.06884 | 1205.83 | 26.91354 | 1205.83 | 32.76531 | 1205.83 | 36.7426 | 1205.83 | -40.2197 |  | 1205.83 | -3.39631 |
| 1206.39 | -5.72326 | 1206.72 | -41.1106 | 1206.5 | 7.6299 | 1206.5 | 26.90495 | 1206.5 | 32.62067 | 1206.5 | 36.79289 | 1206.5 | -40.6543 |  | 1206.5 | -3.69663 |
| 1207.07 | -5.77743 | 1207.4 | -39.8336 | 1207.18 | 7.97208 | 1207.18 | 26.7413 | 1207.18 | 33.6233 | 1207.18 | 36.689 | 1207.18 | -39.946 |  | 1207.18 | -3.21378 |
| 1207.74 | -5.83212 | 1208.07 | -40.6893 | 1207.86 | 9.43528 | 1207.86 | 25.45954 | 1207.86 | 34.52749 | 1207.86 | 35.46701 | 1207.86 | -39.3361 |  | 1207.86 | -1.60989 |
| 1208.42 | -5.88723 | 1208.75 | -40.1641 | 1208.54 | 8.87537 | 1208.54 | 25.48059 | 1208.54 | 33.55687 | 1208.54 | 35.54781 | 1208.54 | -40.6011 |  | 1208.54 | -2.02912 |
| 1209.1 | -5.94247 | 1209.43 | -41.5469 | 1209.21 | 7.99699 | 1209.21 | 25.58617 | 1209.21 | 34.18663 | 1209.21 | 35.71228 | 1209.21 | -40.2613 |  | 1209.21 | -2.7689 |
| 1209.77 | -5.99805 | 1210.11 | -42.9416 | 1209.89 | 7.52574 | 1209.89 | 25.79309 | 1209.89 | 36.0567 | 1209.89 | 35.97896 | 1209.89 | -38.6856 |  | 1209.89 | -3.09947 |
| 1210.45 | -6.05409 | 1210.78 | -43.2261 | 1210.57 | 7.51056 | 1210.57 | 25.03995 | 1210.57 | 33.52695 | 1210.57 | 35.28558 | 1210.57 | -41.5097 |  | 1210.57 | -2.97397 |
| 1211.13 | -6.11091 | 1211.46 | -43.6736 | 1211.25 | 7.15401 | 1211.25 | 23.08929 | 1211.25 | 33.56623 | 1211.25 | 33.39468 | 1211.25 | -41.7647 |  | 1211.25 | -3.18984 |
| 1211.8 | -6.16829 | 1212.14 | -43.4366 | 1211.93 | 6.30176 | 1211.93 | 22.51516 | 1211.93 | 32.92697 | 1211.93 | 32.88031 | 1211.93 | -42.6983 |  | 1211.93 | -3.90141 |
| 1212.48 | -6.22634 | 1212.82 | -43.1148 | 1212.6 | 6.84452 | 1212.6 | 22.03438 | 1212.6 | 33.93436 | 1212.6 | 32.45842 | 1212.6 | -41.9809 |  | 1212.6 | -3.22004 |
| 1213.15 | -6.28498 | 1213.49 | -43.4355 | 1213.28 | 6.95284 | 1213.28 | 21.66142 | 1213.28 | 35.525 | 1213.28 | 32.14521 | 1213.28 | -40.6846 |  | 1213.28 | -2.97105 |
| 1213.83 | -6.34399 | 1214.17 | -46.1328 | 1213.96 | 7.38723 | 1213.96 | 20.65584 | 1213.96 | 35.92465 | 1213.96 | 31.19939 | 1213.96 | -40.5793 |  | 1213.96 | -2.39597 |
| 1214.51 | -6.40316 | 1214.85 | -46.8639 | 1214.63 | 8.0486 | 1214.63 | 20.91294 | 1214.63 | 36.17802 | 1214.63 | 31.51538 | 1214.63 | -40.6159 |  | 1214.63 | -1.59599 |
| 1215.18 | -6.46219 | 1215.52 | -47.2546 | 1215.31 | 9.75868 | 1215.31 | 21.22381 | 1215.31 | 36.58257 | 1215.31 | 31.886 | 1215.31 | -40.5057 |  | 1215.31 | 0.25477 |
| 1215.86 | -6.52095 | 1216.2 | -47.009 | 1215.99 | 11.12543 | 1215.99 | 22.5599 | 1215.99 | 36.07026 | 1215.99 | 33.28186 | 1215.99 | -41.3123 |  | 1215.99 | 1.76219 |
| 1216.53 | -6.5788 | 1216.88 | -45.2967 | 1216.67 | 12.58432 | 1216.67 | 22.26279 | 1216.67 | 36.52609 | 1216.67 | 33.0445 | 1216.67 | -41.1508 |  | 1216.67 | 3.36176 |
| 1217.21 | -6.63605 | 1217.55 | -44.2372 | 1217.34 | 12.86763 | 1217.34 | 22.40322 | 1217.34 | 33.71542 | 1217.34 | 33.24381 | 1217.34 | -44.2515 |  | 1217.34 | 3.78368 |
| 1217.88 | -6.6927 | 1218.23 | -44.3459 | 1218.02 | 13.27121 | 1218.02 | 21.44465 | 1218.02 | 33.2082 | 1218.02 | 32.34501 | 1218.02 | -45.053 |  | 1218.02 | 4.32794 |
| 1218.56 | -6.74835 | 1218.91 | -45.1936 | 1218.7 | 13.1391 | 1218.7 | 21.38119 | 1218.7 | 30.56764 | 1218.7 | 32.34131 | 1218.7 | -47.9879 |  | 1218.7 | 4.3365 |
| 1219.23 | -6.80292 | 1219.58 | -45.3452 | 1219.37 | 13.66747 | 1219.37 | 20.92284 | 1219.37 | 28.78794 | 1219.37 | 31.94184 | 1219.37 | -50.0576 |  | 1219.37 | 5.00349 |
| 1219.91 | -6.8561 | 1220.26 | -46.0294 | 1220.05 | 13.44203 | 1220.05 | 19.49525 | 1220.05 | 27.34385 | 1220.05 | 30.57402 | 1220.05 | -51.796 |  | 1220.05 | 4.91872 |
| 1220.59 | -6.90764 | 1220.94 | -45.8693 | 1220.73 | 14.26147 | 1220.73 | 16.57367 | 1220.73 | 25.96378 | 1220.73 | 27.7122 | 1220.73 | -53.4704 |  | 1220.73 | 5.87884 |
| 1221.26 | -6.95718 | 1221.61 | -44.6303 | 1221.4 | 15.41847 | 1221.4 | 17.9114 | 1221.4 | 24.99839 | 1221.4 | 29.10881 | 1221.4 | -54.7258 |  | 1221.4 | 7.17445 |
| 1221.94 | -7.00443 | 1222.29 | -44.7701 | 1222.08 | 16.7722 | 1222.08 | 18.16877 | 1222.08 | 25.46978 | 1222.08 | 29.42593 | 1222.08 | -54.5487 |  | 1222.08 | 8.66887 |
| 1222.61 | -7.04885 | 1222.96 | -45.5768 | 1222.76 | 16.02849 | 1222.76 | 18.0375 | 1222.76 | 23.08705 | 1222.76 | 29.35443 | 1222.76 | -57.2258 |  | 1222.76 | 8.06583 |
| 1223.29 | -7.09057 | 1223.64 | -48.1652 | 1223.43 | 15.9182 | 1223.43 | 18.56744 | 1223.43 | 23.58714 | 1223.43 | 29.94324 | 1223.43 | -57.0157 |  | 1223.43 | 8.09415 |
| 1223.96 | -7.12922 | 1224.32 | -48.5196 | 1224.11 | 16.2788 | 1224.11 | 18.64872 | 1224.11 | 24.01931 | 1224.11 | 30.08429 | 1224.11 | -56.8779 |  | 1224.11 | 8.59543 |
| 1224.64 | -7.16458 | 1224.99 | -48.7012 | 1224.79 | 17.08212 | 1224.79 | 18.57699 | 1224.79 | 24.58294 | 1224.79 | 30.07232 | 1224.79 | -56.6086 |  | 1224.79 | 9.53943 |
| 1225.31 | -7.19644 | 1225.67 | -49.1757 | 1225.46 | 18.1573 | 1225.46 | 18.87175 | 1225.46 | 24.32626 | 1225.46 | 30.42596 | 1225.46 | -57.1552 |  | 1225.46 | 10.75322 |
| 1225.99 | -7.22436 | 1226.34 | -48.8293 | 1226.14 | 18.87826 | 1226.14 | 19.38112 | 1226.14 | 24.52626 | 1226.14 | 30.99509 | 1226.14 | -57.2496 |  | 1226.14 | 11.61485 |
| 1226.66 | -7.24841 | 1227.02 | -48.9513 | 1226.81 | 17.59109 | 1226.81 | 18.89333 | 1226.81 | 23.82879 | 1226.81 | 30.56619 | 1226.81 | -58.237 |  | 1226.81 | 10.46629 |
| 1227.34 | -7.26866 | 1227.7 | -50.2235 | 1227.49 | 15.93792 | 1227.49 | 17.61624 | 1227.49 | 23.15487 | 1227.49 | 29.34885 | 1227.49 | -59.2053 |  | 1227.49 | 8.95381 |
| 1228.01 | -7.2848 | 1228.37 | -50.229 | 1228.17 | 17.00631 | 1228.17 | 17.43494 | 1228.17 | 23.63751 | 1228.17 | 29.22732 | 1228.17 | -59.017 |  | 1228.17 | 10.16288 |
| 1228.68 | -7.29673 | 1229.05 | -50.8249 | 1228.84 | 18.29814 | 1228.84 | 14.35767 | 1228.84 | 22.3768 | 1228.84 | 26.20892 | 1228.84 | -60.5677 |  | 1228.84 | 11.59332 |
| 1229.36 | -7.30418 | 1229.72 | -51.0746 | 1229.52 | 18.03063 | 1229.52 | 13.64709 | 1229.52 | 21.95364 | 1229.52 | 25.5581 | 1229.52 | -61.2852 |  | 1229.52 | 11.46648 |
| 1230.03 | -7.30743 | 1230.4 | -49.4591 | 1230.19 | 17.85342 | 1230.19 | 11.91993 | 1230.19 | 24.63518 | 1230.19 | 23.88983 | 1230.19 | -58.8936 |  | 1230.19 | 11.42788 |
| 1230.71 | -7.30658 | 1231.07 | -47.4189 | 1230.87 | 17.31473 | 1230.87 | 12.20562 | 1230.87 | 24.41614 | 1230.87 | 24.23528 | 1230.87 | -59.407 |  | 1230.87 | 11.02987 |
| 1231.38 | -7.30153 | 1231.75 | -48.0457 | 1231.54 | 17.1677 | 1231.54 | 12.70898 | 1231.54 | 24.0911 | 1231.54 | 24.79752 | 1231.54 | -60.022 |  | 1231.54 | 11.02145 |
| 1232.06 | -7.29251 | 1232.42 | -48.2471 | 1232.22 | 15.03568 | 1232.22 | 11.07565 | 1232.22 | 23.11187 | 1232.22 | 23.22396 | 1232.22 | -61.2956 |  | 1232.22 | 9.03011 |
| 1232.73 | -7.27952 | 1233.1 | -48.3597 | 1232.9 | 16.22639 | 1232.9 | 11.3746 | 1232.9 | 23.46194 | 1232.9 | 23.58267 | 1232.9 | -61.2398 |  | 1232.9 | 10.36149 |
| 1233.41 | -7.26249 | 1233.77 | -48.5684 | 1233.57 | 16.88659 | 1233.57 | 9.12808 | 1233.57 | 22.54032 | 1233.57 | 21.39503 | 1233.57 | -62.4515 |  | 1233.57 | 11.16031 |
| 1234.08 | -7.24151 | 1234.45 | -48.5067 | 1234.25 | 18.00865 | 1234.25 | 9.70716 | 1234.25 | 21.81264 | 1234.25 | 22.03386 | 1234.25 | -63.4735 |  | 1234.25 | 12.42305 |
| 1234.75 | -7.21643 | 1235.12 | -48.2426 | 1234.92 | 16.79494 | 1234.92 | 10.41083 | 1234.92 | 19.32848 | 1234.92 | 22.79642 | 1234.92 | -66.2476 |  | 1234.92 | 11.34794 |
| 1235.43 | -7.18701 | 1235.8 | -49.7289 | 1235.6 | 17.22345 | 1235.6 | 10.76944 | 1235.6 | 18.39893 | 1235.6 | 23.21478 | 1235.6 | -67.4715 |  | 1235.6 | 11.91714 |
| 1236.1 | -7.15303 | 1236.47 | -49.607 | 1236.27 | 18.77972 | 1236.27 | 10.37539 | 1236.27 | 20.20877 | 1236.27 | 22.87962 | 1236.27 | -65.9517 |  | 1236.27 | 13.61201 |
| 1236.77 | -7.11478 | 1237.15 | -50.9048 | 1236.95 | 19.22098 | 1236.95 | 11.23164 | 1236.95 | 20.22197 | 1236.95 | 23.79563 | 1236.95 | -66.2328 |  | 1236.95 | 14.19395 |
| 1237.45 | -7.07263 | 1237.82 | -51.554 | 1237.62 | 19.2635 | 1237.62 | 11.7834 | 1237.62 | 21.45661 | 1237.62 | 24.40627 | 1237.62 | -65.2882 |  | 1237.62 | 14.37508 |
| 1238.12 | -7.0271 | 1238.5 | -52.3152 | 1238.3 | 20.85905 | 1238.3 | 12.60958 | 1238.3 | 22.90989 | 1238.3 | 25.29221 | 1238.3 | -64.1292 |  | 1238.3 | 16.11131 |
| 1238.8 | -6.97873 | 1239.17 | -52.3763 | 1238.97 | 19.74981 | 1238.97 | 12.08703 | 1238.97 | 20.10414 | 1238.97 | 24.82854 | 1238.97 | -67.2249 |  | 1238.97 | 15.14068 |
| 1239.47 | -6.92777 | 1239.85 | -52.7739 | 1239.65 | 19.42437 | 1239.65 | 11.51627 | 1239.65 | 19.7832 | 1239.65 | 24.31754 | 1239.65 | -67.8402 |  | 1239.65 | 14.95592 |
| 1240.14 | -6.87462 | 1240.52 | -53.0328 | 1240.32 | 19.34491 | 1240.32 | 11.72266 | 1240.32 | 19.54264 | 1240.32 | 24.58281 | 1240.32 | -68.3708 |  | 1240.32 | 15.01507 |
| 1240.82 | -6.82009 | 1241.19 | -52.9161 | 1241 | 19.54927 | 1241 | 11.19131 | 1241 | 18.92915 | 1241 | 24.11123 | 1241 | -69.2786 |  | 1241 | 15.36011 |
| 1241.49 | -6.76423 | 1241.87 | -53.6051 | 1241.67 | 20.11293 | 1241.67 | 10.66351 | 1241.67 | 17.90535 | 1241.67 | 23.64231 | 1241.67 | -70.5924 |  | 1241.67 | 16.06238 |
| 1242.16 | -6.70719 | 1242.54 | -54.2888 | 1242.34 | 18.75111 | 1242.34 | 9.95139 | 1242.34 | 17.98566 | 1242.34 | 22.98908 | 1242.34 | -70.8021 |  | 1242.34 | 14.83917 |
| 1242.84 | -6.64925 | 1243.22 | -53.1116 | 1243.02 | 18.88663 | 1243.02 | 9.24409 | 1243.02 | 18.9454 | 1243.02 | 22.34153 | 1243.02 | -70.1367 |  | 1243.02 | 15.11536 |
| 1243.51 | -6.59056 | 1243.89 | -52.918 | 1243.69 | 20.32596 | 1243.69 | 8.57347 | 1243.69 | 18.26129 | 1243.69 | 21.72979 | 1243.69 | -71.1108 |  | 1243.69 | 16.69331 |
| 1244.18 | -6.53154 | 1244.56 | -51.3711 | 1244.37 | 19.4746 | 1244.37 | 6.03491 | 1244.37 | 17.33603 | 1244.37 | 19.25099 | 1244.37 | -72.3304 |  | 1244.37 | 15.98262 |
| 1244.85 | -6.4727 | 1245.24 | -51.8825 | 1245.04 | 19.92412 | 1245.04 | 5.32292 | 1245.04 | 17.03525 | 1245.04 | 18.59788 | 1245.04 | -72.9211 |  | 1245.04 | 16.57076 |
| 1245.53 | -6.41457 | 1245.91 | -52.2876 | 1245.72 | 20.15039 | 1245.72 | 5.79997 | 1245.72 | 16.21811 | 1245.72 | 19.1347 | 1245.72 | -74.0326 |  | 1245.72 | 16.9377 |
| 1246.2 | -6.3575 | 1246.59 | -52.4244 | 1246.39 | 19.68853 | 1246.39 | 5.11418 | 1246.39 | 13.91959 | 1246.39 | 18.50778 | 1246.39 | -76.6211 |  | 1246.39 | 16.61445 |
| 1246.87 | -6.30151 | 1247.26 | -52.7324 | 1247.06 | 18.07645 | 1247.06 | 5.80654 | 1247.06 | 14.28801 | 1247.06 | 19.25903 | 1247.06 | -76.5427 |  | 1247.06 | 15.14099 |
| 1247.55 | -6.24692 | 1247.93 | -51.8862 | 1247.74 | 17.76742 | 1247.74 | 5.20379 | 1247.74 | 11.71577 | 1247.74 | 18.71604 | 1247.74 | -79.4093 |  | 1247.74 | 14.97264 |
| 1248.22 | -6.19378 | 1248.61 | -51.3059 | 1248.41 | 16.68025 | 1248.41 | 4.28832 | 1248.41 | 12.36871 | 1248.41 | 17.85945 | 1248.41 | -79.0463 |  | 1248.41 | 14.02407 |
| 1248.89 | -6.14226 | 1249.28 | -51.0635 | 1249.09 | 16.29767 | 1249.09 | 3.98216 | 1249.09 | 10.79303 | 1249.09 | 17.61305 | 1249.09 | -80.9163 |  | 1249.09 | 13.78217 |
| 1249.56 | -6.09249 | 1249.95 | -50.0768 | 1249.76 | 14.87597 | 1249.76 | 2.11484 | 1249.76 | 7.14743 | 1249.76 | 15.80462 | 1249.76 | -84.8519 |  | 1249.76 | 12.49908 |
| 1250.24 | -6.04463 | 1250.63 | -50.9886 | 1250.43 | 12.88582 | 1250.43 | 0.82137 | 1250.43 | 5.61545 | 1250.43 | 14.57003 | 1250.43 | -86.6739 |  | 1250.43 | 10.64754 |
| 1250.91 | -5.99892 | 1251.3 | -51.6733 | 1251.11 | 11.31558 | 1251.11 | 0.97985 | 1251.11 | 3.83437 | 1251.11 | 14.78826 | 1251.11 | -88.7493 |  | 1251.11 | 9.21798 |
| 1251.58 | -5.95533 | 1251.97 | -52.5615 | 1251.78 | 10.79935 | 1251.78 | 0.24442 | 1251.78 | 4.4971 | 1251.78 | 14.11172 | 1251.78 | -88.3766 |  | 1251.78 | 8.84036 |
| 1252.25 | -5.91452 | 1252.65 | -54.5117 | 1252.45 | 10.6494 | 1252.45 | -1.23729 | 1252.45 | 1.94178 | 1252.45 | 12.68889 | 1252.45 | -91.2219 |  | 1252.45 | 8.82901 |
| 1252.93 | -5.87678 | 1253.32 | -54.5323 | 1253.13 | 9.53814 | 1253.13 | -1.07857 | 1253.13 | 2.55265 | 1253.13 | 12.90737 | 1253.13 | -90.9054 |  | 1253.13 | 7.85843 |
| 1253.6 | -5.84193 | 1253.99 | -54.967 | 1253.8 | 10.58071 | 1253.8 | -1.20918 | 1253.8 | 3.16958 | 1253.8 | 12.83565 | 1253.8 | -90.5784 |  | 1253.8 | 9.03962 |
| 1254.27 | -5.81033 | 1254.67 | -56.0959 | 1254.47 | 11.12386 | 1254.47 | 0.08339 | 1254.47 | 1.91327 | 1254.47 | 14.19169 | 1254.47 | -92.1247 |  | 1254.47 | 9.72138 |
| 1254.94 | -5.78225 | 1255.34 | -55.7728 | 1255.15 | 10.59456 | 1255.15 | 0.65056 | 1255.15 | 0.85257 | 1255.15 | 14.88742 | 1255.15 | -93.4798 |  | 1255.15 | 9.33276 |
| 1255.61 | -5.75795 | 1256.01 | -56.9134 | 1255.82 | 9.3581 | 1255.82 | 0.07779 | 1255.82 | 2.63548 | 1255.82 | 14.44131 | 1255.82 | -91.9869 |  | 1255.82 | 8.23491 |
| 1256.29 | -5.73726 | 1256.68 | -56.3015 | 1256.49 | 10.12184 | 1256.49 | 0.36462 | 1256.49 | 1.3523 | 1256.49 | 14.85481 | 1256.49 | -93.56 |  | 1256.49 | 9.13725 |
| 1256.96 | -5.72 | 1257.36 | -56.7109 | 1257.17 | 9.10741 | 1257.17 | -0.09503 | 1257.17 | 0.91884 | 1257.17 | 14.52373 | 1257.17 | -94.2878 |  | 1257.17 | 8.2635 |
| 1257.63 | -5.70588 | 1258.03 | -55.4693 | 1257.84 | 9.93544 | 1257.84 | -0.56082 | 1257.84 | -1.11973 | 1257.84 | 14.1846 | 1257.84 | -96.6164 |  | 1257.84 | 9.23014 |
| 1258.3 | -5.69494 | 1258.7 | -56.5302 | 1258.51 | 7.98541 | 1258.51 | -0.98728 | 1258.51 | -1.38253 | 1258.51 | 13.88481 | 1258.51 | -97.1692 |  | 1258.51 | 7.41872 |
| 1258.97 | -5.68708 | 1259.38 | -56.9574 | 1259.19 | 6.03135 | 1259.19 | -0.36582 | 1259.19 | -2.23492 | 1259.19 | 14.63483 | 1259.19 | -98.3159 |  | 1259.19 | 5.60534 |
| 1259.64 | -5.68217 | 1260.05 | -54.5287 | 1259.86 | 6.12115 | 1259.86 | 1.68545 | 1259.86 | -2.11859 | 1259.86 | 16.81276 | 1259.86 | -98.4896 |  | 1259.86 | 5.83375 |
| 1260.31 | -5.68013 | 1260.72 | -53.7584 | 1260.53 | 5.94093 | 1260.53 | 0.97997 | 1260.53 | 0.4839 | 1260.53 | 16.23395 | 1260.53 | -96.1771 |  | 1260.53 | 5.79214 |
| 1260.99 | -5.68052 | 1261.39 | -53.5631 | 1261.2 | 6.0856 | 1261.2 | 1.67744 | 1261.2 | -0.84046 | 1261.2 | 17.05808 | 1261.2 | -97.7914 |  | 1261.2 | 6.07543 |
| 1261.66 | -5.6833 | 1262.06 | -51.6519 | 1261.88 | 6.808 | 1261.88 | 2.8147 | 1261.88 | 0.51841 | 1261.88 | 18.32391 | 1261.88 | -96.7269 |  | 1261.88 | 6.9385 |
| 1262.33 | -5.68852 | 1262.74 | -52.3371 | 1262.55 | 7.74737 | 1262.55 | 4.35935 | 1262.55 | -0.47822 | 1262.55 | 19.99522 | 1262.55 | -98.0135 |  | 1262.55 | 8.01648 |
| 1263 | -5.69626 | 1263.41 | -53.4342 | 1263.22 | 7.92711 | 1263.22 | 4.98294 | 1263.22 | 1.11079 | 1263.22 | 20.74548 | 1263.22 | -96.3134 |  | 1263.22 | 8.33483 |
| 1263.67 | -5.70655 | 1264.08 | -54.5436 | 1263.89 | 7.79528 | 1263.89 | 4.35064 | 1263.89 | 1.65135 | 1263.89 | 20.23985 | 1263.89 | -95.5348 |  | 1263.89 | 8.34161 |
| 1264.34 | -5.71914 | 1264.75 | -54.1229 | 1264.57 | 7.22138 | 1264.57 | 6.03019 | 1264.57 | -0.4636 | 1264.57 | 22.04795 | 1264.57 | -97.4082 |  | 1264.57 | 7.90839 |
| 1265.01 | -5.73371 | 1265.42 | -54.73 | 1265.24 | 6.4515 | 1265.24 | 6.01017 | 1265.24 | 0.08215 | 1265.24 | 22.1546 | 1265.24 | -96.6245 |  | 1265.24 | 7.27712 |
| 1265.68 | -5.75023 | 1266.1 | -53.7197 | 1265.91 | 6.3724 | 1265.91 | 7.69643 | 1265.91 | 0.65026 | 1265.91 | 23.96753 | 1265.91 | -95.8184 |  | 1265.91 | 7.33663 |
| 1266.35 | -5.76844 | 1266.77 | -53.4825 | 1266.58 | 7.18367 | 1266.58 | 8.09281 | 1266.58 | 3.06257 | 1266.58 | 24.49058 | 1266.58 | -93.1681 |  | 1266.58 | 8.28651 |
| 1267.03 | -5.78802 | 1267.44 | -52.7296 | 1267.25 | 5.81259 | 1267.25 | 8.76115 | 1267.25 | 1.83312 | 1267.25 | 25.28559 | 1267.25 | -94.1595 |  | 1267.25 | 7.05404 |
| 1267.7 | -5.80882 | 1268.11 | -53.8642 | 1267.93 | 6.39356 | 1267.93 | 11.39525 | 1267.93 | 2.856 | 1267.93 | 28.04825 | 1267.93 | -92.8951 |  | 1267.93 | 7.77569 |
| 1268.37 | -5.83066 | 1268.78 | -54.5532 | 1268.6 | 5.64756 | 1268.6 | 10.52744 | 1268.6 | 2.36742 | 1268.6 | 27.3071 | 1268.6 | -93.1457 |  | 1268.6 | 7.1683 |
| 1269.04 | -5.85327 | 1269.45 | -55.5738 | 1269.27 | 8.33784 | 1269.27 | 11.73669 | 1269.27 | 3.26335 | 1269.27 | 28.64302 | 1269.27 | -92.0118 |  | 1269.27 | 9.99718 |
| 1269.71 | -5.8768 | 1270.13 | -56.0728 | 1269.94 | 7.8038 | 1269.94 | 11.69751 | 1269.94 | 3.51046 | 1269.94 | 28.7305 | 1269.94 | -91.5267 |  | 1269.94 | 9.60176 |
| 1270.38 | -5.90122 | 1270.8 | -55.203 | 1270.61 | 7.19661 | 1270.61 | 12.45021 | 1270.61 | 2.96707 | 1270.61 | 29.60987 | 1270.61 | -91.832 |  | 1270.61 | 9.13317 |
| 1271.05 | -5.92628 | 1271.47 | -57.2667 | 1271.28 | 8.06118 | 1271.28 | 12.87781 | 1271.28 | 2.51035 | 1271.28 | 30.16414 | 1271.28 | -92.0508 |  | 1271.28 | 10.13635 |
| 1271.72 | -5.95203 | 1272.14 | -58.4404 | 1271.96 | 7.16878 | 1271.96 | 13.97804 | 1271.96 | 1.63184 | 1271.96 | 31.39292 | 1271.96 | -92.6877 |  | 1271.96 | 9.38463 |
| 1272.39 | -5.97807 | 1272.81 | -59.0732 | 1272.63 | 5.66431 | 1272.63 | 12.94635 | 1272.63 | 1.7354 | 1272.63 | 30.4879 | 1272.63 | -92.3462 |  | 1272.63 | 8.01878 |
| 1273.06 | -6.00419 | 1273.48 | -59.5242 | 1273.3 | 5.35318 | 1273.3 | 13.93721 | 1273.3 | 4.39896 | 1273.3 | 31.60543 | 1273.3 | -89.4446 |  | 1273.3 | 7.84625 |
| 1273.73 | -6.03045 | 1274.15 | -59.6179 | 1273.97 | 5.17126 | 1273.97 | 16.21905 | 1273.97 | 3.20037 | 1273.97 | 34.01394 | 1273.97 | -90.4052 |  | 1273.97 | 7.80294 |
| 1274.4 | -6.05664 | 1274.82 | -61.5054 | 1274.64 | 4.89011 | 1274.64 | 16.79612 | 1274.64 | 2.94324 | 1274.64 | 34.71767 | 1274.64 | -90.4243 |  | 1274.64 | 7.6604 |
| 1275.07 | -6.0828 | 1275.49 | -61.449 | 1275.31 | 4.74014 | 1275.31 | 15.99553 | 1275.31 | 4.4316 | 1275.31 | 34.04376 | 1275.31 | -88.698 |  | 1275.31 | 7.64904 |
| 1275.74 | -6.1091 | 1276.17 | -60.7226 | 1275.98 | 3.68604 | 1275.98 | 15.62142 | 1275.98 | 4.09035 | 1275.98 | 33.79631 | 1275.98 | -88.8012 |  | 1275.98 | 6.73356 |
| 1276.41 | -6.13345 | 1276.84 | -61.2627 | 1276.66 | 5.1583 | 1276.66 | 15.6922 | 1276.66 | 5.52995 | 1276.66 | 33.99565 | 1276.66 | -87.1201 |  | 1276.66 | 8.34649 |
| 1277.08 | -6.15573 | 1277.51 | -61.0864 | 1277.33 | 4.09732 | 1277.33 | 17.31546 | 1277.33 | 6.82683 | 1277.33 | 35.74558 | 1277.33 | -85.5852 |  | 1277.33 | 7.42412 |
| 1277.75 | -6.17604 | 1278.18 | -60.6989 | 1278 | 3.78027 | 1278 | 17.66637 | 1278 | 7.86371 | 1278 | 36.22315 | 1278 | -84.3103 |  | 1278 | 7.24568 |
| 1278.42 | -6.19415 | 1278.85 | -59.3811 | 1278.67 | 6.28891 | 1278.67 | 19.48845 | 1278.67 | 7.20373 | 1278.67 | 38.17191 | 1278.67 | -84.7323 |  | 1278.67 | 9.89293 |
| 1279.09 | -6.21007 | 1279.52 | -58.3815 | 1279.34 | 5.49713 | 1279.34 | 21.64125 | 1279.34 | 7.81776 | 1279.34 | 40.45137 | 1279.34 | -83.8803 |  | 1279.34 | 9.23976 |
| 1279.76 | -6.22363 | 1280.19 | -58.8889 | 1280.01 | 6.89281 | 1280.01 | 22.58345 | 1280.01 | 9.30708 | 1280.01 | 41.52024 | 1280.01 | -82.153 |  | 1280.01 | 10.77405 |
| 1280.43 | -6.23499 | 1280.86 | -58.5205 | 1280.68 | 8.20162 | 1280.68 | 22.5986 | 1280.68 | 11.57386 | 1280.68 | 41.66206 | 1280.68 | -79.6482 |  | 1280.68 | 12.22147 |
| 1281.1 | -6.2443 | 1281.53 | -57.9997 | 1281.35 | 10.06749 | 1281.35 | 22.97395 | 1281.35 | 12.73867 | 1281.35 | 42.16407 | 1281.35 | -78.2454 |  | 1281.35 | 14.22595 |
| 1281.77 | -6.25135 | 1282.2 | -58.0616 | 1282.02 | 11.79609 | 1282.02 | 23.17392 | 1282.02 | 14.9171 | 1282.02 | 42.49071 | 1282.02 | -75.829 |  | 1282.02 | 16.09316 |
| 1282.43 | -6.25592 | 1282.87 | -57.7463 | 1282.69 | 13.16957 | 1282.69 | 25.69421 | 1282.69 | 14.53661 | 1282.69 | 45.13767 | 1282.69 | -75.9715 |  | 1282.69 | 17.60525 |
| 1283.1 | -6.25785 | 1283.54 | -58.8464 | 1283.36 | 14.37619 | 1283.36 | 26.8945 | 1283.36 | 16.07866 | 1283.36 | 46.46463 | 1283.36 | -74.1914 |  | 1283.36 | 18.95048 |
| 1283.77 | -6.25727 | 1284.21 | -57.8155 | 1284.03 | 14.49124 | 1284.03 | 29.15225 | 1284.03 | 17.63346 | 1284.03 | 48.84904 | 1284.03 | -72.3986 |  | 1284.03 | 19.20414 |
| 1284.44 | -6.25415 | 1284.88 | -57.823 | 1284.7 | 15.51355 | 1284.7 | 30.82077 | 1284.7 | 19.47532 | 1284.7 | 50.64423 | 1284.7 | -70.3188 |  | 1284.7 | 20.36506 |
| 1285.11 | -6.24845 | 1285.55 | -59.16 | 1285.37 | 16.54721 | 1285.37 | 32.48903 | 1285.37 | 22.20158 | 1285.37 | 52.43915 | 1285.37 | -67.3545 |  | 1285.37 | 21.53733 |
| 1285.78 | -6.24026 | 1286.22 | -59.1194 | 1286.04 | 17.73832 | 1286.04 | 33.72728 | 1286.04 | 23.84666 | 1286.04 | 53.80408 | 1286.04 | -65.4714 |  | 1286.04 | 22.86705 |
| 1286.45 | -6.22971 | 1286.89 | -61.1275 | 1286.71 | 17.46981 | 1286.71 | 34.96468 | 1286.71 | 26.57615 | 1286.71 | 55.16814 | 1286.71 | -62.5039 |  | 1286.71 | 22.73715 |
| 1287.12 | -6.217 | 1287.56 | -60.0732 | 1287.38 | 18.23933 | 1287.38 | 36.57365 | 1287.38 | 28.47701 | 1287.38 | 56.90378 | 1287.38 | -60.3651 |  | 1287.38 | 23.64528 |
| 1287.79 | -6.2022 | 1288.23 | -60.8466 | 1288.05 | 17.74455 | 1288.05 | 36.543 | 1288.05 | 30.38513 | 1288.05 | 56.9998 | 1288.05 | -58.219 |  | 1288.05 | 23.2891 |
| 1288.45 | -6.18491 | 1288.9 | -61.6142 | 1288.72 | 17.48976 | 1288.72 | 36.24001 | 1288.72 | 30.5803 | 1288.72 | 56.82347 | 1288.72 | -57.7858 |  | 1288.72 | 23.17292 |
| 1289.12 | -6.16516 | 1289.57 | -61.8156 | 1289.39 | 18.12142 | 1289.39 | 36.89537 | 1289.39 | 32.37106 | 1289.39 | 57.6055 | 1289.39 | -55.757 |  | 1289.39 | 23.9432 |
| 1289.79 | -6.14333 | 1290.24 | -62.3306 | 1290.06 | 18.75328 | 1290.06 | 37.02779 | 1290.06 | 31.93475 | 1290.06 | 57.86459 | 1290.06 | -55.9553 |  | 1290.06 | 24.71367 |
| 1290.46 | -6.11958 | 1290.91 | -61.3914 | 1290.73 | 16.81199 | 1290.73 | 37.62504 | 1290.73 | 32.27717 | 1290.73 | 58.5885 | 1290.73 | -55.3749 |  | 1290.73 | 22.91098 |
| 1291.13 | -6.09385 | 1291.58 | -62.0566 | 1291.4 | 17.46618 | 1291.4 | 37.68444 | 1291.4 | 33.93193 | 1291.4 | 58.77457 | 1291.4 | -53.4822 |  | 1291.4 | 23.70379 |
| 1291.8 | -6.06622 | 1292.25 | -63.0676 | 1292.07 | 17.8094 | 1292.07 | 38.14914 | 1292.07 | 34.14984 | 1292.07 | 59.36594 | 1292.07 | -53.0263 |  | 1292.07 | 24.18561 |
| 1292.46 | -6.03648 | 1292.91 | -62.0768 | 1292.74 | 19.83045 | 1292.74 | 37.99462 | 1292.74 | 35.82519 | 1292.74 | 59.33809 | 1292.74 | -51.1129 |  | 1292.74 | 26.34528 |
| 1293.13 | -6.00459 | 1293.58 | -61.9981 | 1293.41 | 23.36112 | 1293.41 | 37.81148 | 1293.41 | 35.56976 | 1293.41 | 59.28161 | 1293.41 | -51.1303 |  | 1293.41 | 30.01455 |
| 1293.8 | -5.97075 | 1294.25 | -60.7358 | 1294.08 | 23.95626 | 1294.08 | 35.92759 | 1294.08 | 38.25804 | 1294.08 | 57.52439 | 1294.08 | -48.2041 |  | 1294.08 | 30.7483 |
| 1294.47 | -5.93501 | 1294.92 | -61.7526 | 1294.75 | 25.06748 | 1294.75 | 37.20665 | 1294.75 | 36.6024 | 1294.75 | 58.93012 | 1294.75 | -49.6217 |  | 1294.75 | 31.99813 |
| 1295.14 | -5.8973 | 1295.59 | -61.1351 | 1295.42 | 26.84752 | 1295.42 | 37.50904 | 1295.42 | 39.18637 | 1295.42 | 59.35918 | 1295.42 | -46.7997 |  | 1295.42 | 33.91678 |
| 1295.8 | -5.85775 | 1296.26 | -60.5493 | 1296.09 | 28.33972 | 1296.09 | 37.22849 | 1296.09 | 40.67837 | 1296.09 | 59.20529 | 1296.09 | -45.0697 |  | 1296.09 | 35.54759 |
| 1296.47 | -5.81613 | 1296.93 | -60.0982 | 1296.76 | 29.4219 | 1296.76 | 36.79924 | 1296.76 | 41.37576 | 1296.76 | 58.90271 | 1296.76 | -44.1344 |  | 1296.76 | 36.76838 |
| 1297.14 | -5.77234 | 1297.6 | -59.8747 | 1297.43 | 30.07231 | 1297.43 | 37.19959 | 1297.43 | 40.96707 | 1297.43 | 59.42973 | 1297.43 | -44.3051 |  | 1297.43 | 37.55741 |
| 1297.81 | -5.72687 | 1298.27 | -59.9946 | 1298.1 | 30.28488 | 1298.1 | 38.20681 | 1298.1 | 42.26329 | 1298.1 | 60.56362 | 1298.1 | -42.7708 |  | 1298.1 | 37.90859 |
| 1298.48 | -5.6801 | 1298.93 | -60.3567 | 1298.77 | 31.03942 | 1298.77 | 38.26913 | 1298.77 | 43.67754 | 1298.77 | 60.7526 | 1298.77 | -41.1186 |  | 1298.77 | 38.80173 |
| 1299.14 | -5.63214 | 1299.6 | -58.171 | 1299.43 | 33.73247 | 1299.43 | 39.62365 | 1299.43 | 44.64798 | 1299.43 | 62.2319 | 1299.43 | -39.9137 |  | 1299.43 | 41.63133 |
| 1299.81 | -5.58263 | 1300.27 | -56.8034 | 1300.1 | 34.47503 | 1300.1 | 38.63432 | 1300.1 | 44.76487 | 1300.1 | 61.36924 | 1300.1 | -39.5588 |  | 1300.1 | 42.51249 |
| 1300.48 | -5.5316 | 1300.94 | -56.2198 | 1300.77 | 35.38425 | 1300.77 | 39.46617 | 1300.77 | 43.42961 | 1300.77 | 62.32776 | 1300.77 | -40.6561 |  | 1300.77 | 43.56032 |
| 1301.15 | -5.47906 | 1301.61 | -55.9657 | 1301.44 | 35.96188 | 1301.44 | 40.24285 | 1301.44 | 44.95424 | 1301.44 | 63.2311 | 1301.44 | -38.8935 |  | 1301.44 | 44.27657 |
| 1301.81 | -5.42481 | 1302.28 | -55.2728 | 1302.11 | 35.38658 | 1302.11 | 40.40541 | 1302.11 | 45.50475 | 1302.11 | 63.52033 | 1302.11 | -38.1049 |  | 1302.11 | 43.83987 |
| 1302.48 | -5.36887 | 1302.94 | -55.2152 | 1302.78 | 35.33107 | 1302.78 | 40.50777 | 1302.78 | 46.62291 | 1302.78 | 63.74936 | 1302.78 | -36.7488 |  | 1302.78 | 43.92298 |
| 1303.15 | -5.31137 | 1303.61 | -55.6087 | 1303.44 | 33.99509 | 1303.44 | 39.54046 | 1303.44 | 47.92462 | 1303.44 | 62.90682 | 1303.44 | -35.2126 |  | 1303.44 | 42.72354 |
| 1303.81 | -5.25243 | 1304.28 | -55.6776 | 1304.11 | 33.49369 | 1304.11 | 39.53666 | 1304.11 | 48.39561 | 1304.11 | 63.0297 | 1304.11 | -34.5036 |  | 1304.11 | 42.36074 |
| 1304.48 | -5.19249 | 1304.95 | -55.2504 | 1304.78 | 33.61405 | 1304.78 | 39.63797 | 1304.78 | 49.61504 | 1304.78 | 63.25767 | 1304.78 | -33.0462 |  | 1304.78 | 42.61971 |
| 1305.15 | -5.13222 | 1305.62 | -54.8501 | 1305.45 | 32.30753 | 1305.45 | 39.48548 | 1305.45 | 49.49136 | 1305.45 | 63.23184 | 1305.45 | -32.9319 |  | 1305.45 | 41.4518 |
| 1305.82 | -5.07185 | 1306.28 | -54.2993 | 1306.12 | 34.14866 | 1306.12 | 38.56122 | 1306.12 | 47.9841 | 1306.12 | 62.43425 | 1306.12 | -34.2012 |  | 1306.12 | 43.43154 |
| 1306.48 | -5.01162 | 1306.95 | -56.794 | 1306.79 | 34.77508 | 1306.79 | 38.53363 | 1306.79 | 45.91345 | 1306.79 | 62.53333 | 1306.79 | -36.0338 |  | 1306.79 | 44.19657 |
| 1307.15 | -4.95151 | 1307.62 | -57.5834 | 1307.45 | 35.96081 | 1307.45 | 38.66981 | 1307.45 | 44.37345 | 1307.45 | 62.79429 | 1307.45 | -37.3394 |  | 1307.45 | 45.51884 |
| 1307.82 | -4.89156 | 1308.29 | -56.9636 | 1308.12 | 37.21584 | 1308.12 | 37.38411 | 1308.12 | 45.91985 | 1308.12 | 61.63525 | 1308.12 | -35.555 |  | 1308.12 | 46.91248 |
| 1308.48 | -4.8321 | 1308.95 | -57.6808 | 1308.79 | 37.67283 | 1308.79 | 38.63762 | 1308.79 | 46.5264 | 1308.79 | 63.01543 | 1308.79 | -34.7104 |  | 1308.79 | 47.50809 |
| 1309.15 | -4.77344 | 1309.62 | -57.9166 | 1309.46 | 38.36314 | 1309.46 | 39.91792 | 1309.46 | 44.43141 | 1309.46 | 64.4224 | 1309.46 | -36.5674 |  | 1309.46 | 48.337 |
| 1309.82 | -4.71556 | 1310.29 | -58.4186 | 1310.13 | 38.61953 | 1310.13 | 41.37057 | 1310.13 | 45.13323 | 1310.13 | 66.00171 | 1310.13 | -35.6276 |  | 1310.13 | 48.732 |
| 1310.48 | -4.65858 | 1310.96 | -59.3356 | 1310.79 | 39.14092 | 1310.79 | 41.49903 | 1310.79 | 43.97601 | 1310.79 | 66.25495 | 1310.79 | -36.5504 |  | 1310.79 | 49.38994 |
| 1311.15 | -4.60264 | 1311.63 | -59.3684 | 1311.46 | 40.80729 | 1311.46 | 39.92043 | 1311.46 | 42.3686 | 1311.46 | 64.80302 | 1311.46 | -37.9198 |  | 1311.46 | 51.19492 |
| 1311.81 | -4.54789 | 1312.29 | -60.3447 | 1312.13 | 40.00895 | 1312.13 | 40.20654 | 1312.13 | 42.22408 | 1312.13 | 65.21579 | 1312.13 | -37.8263 |  | 1312.13 | 50.53519 |
| 1312.48 | -4.49431 | 1312.96 | -61.0625 | 1312.8 | 39.71844 | 1312.8 | 40.54825 | 1312.8 | 42.07077 | 1312.8 | 65.68418 | 1312.8 | -37.7416 |  | 1312.8 | 50.38329 |
| 1313.15 | -4.44185 | 1313.63 | -61.2102 | 1313.46 | 39.66507 | 1313.46 | 39.11637 | 1313.46 | 41.24155 | 1313.46 | 64.37707 | 1313.46 | -38.3364 |  | 1313.46 | 50.46646 |
| 1313.81 | -4.39039 | 1314.29 | -61.5262 | 1314.13 | 39.46686 | 1314.13 | 39.30573 | 1314.13 | 39.22971 | 1314.13 | 64.6931 | 1314.13 | -40.1103 |  | 1314.13 | 50.40685 |
| 1314.48 | -4.33998 | 1314.96 | -63.0888 | 1314.8 | 38.26098 | 1314.8 | 38.36698 | 1314.8 | 39.12045 | 1314.8 | 63.88102 | 1314.8 | -39.9815 |  | 1314.8 | 49.33958 |
| 1315.14 | -4.2909 | 1315.63 | -65.6665 | 1315.47 | 37.11566 | 1315.47 | 37.45392 | 1315.47 | 38.53231 | 1315.47 | 63.09462 | 1315.47 | -40.3317 |  | 1315.47 | 48.33288 |
| 1315.81 | -4.24318 | 1316.29 | -65.327 | 1316.13 | 35.36083 | 1316.13 | 36.49522 | 1316.13 | 38.5709 | 1316.13 | 62.2607 | 1316.13 | -40.0586 |  | 1316.13 | 46.71459 |
| 1316.48 | -4.19667 | 1316.96 | -65.7062 | 1316.8 | 34.54686 | 1316.8 | 36.82686 | 1316.8 | 38.41933 | 1316.8 | 62.71901 | 1316.8 | -39.9722 |  | 1316.8 | 46.03923 |
| 1317.14 | -4.15129 | 1317.63 | -66.506 | 1317.47 | 33.50699 | 1317.47 | 35.66137 | 1317.47 | 37.587 | 1317.47 | 61.68019 | 1317.47 | -40.5665 |  | 1317.47 | 45.13797 |
| 1317.81 | -4.10692 | 1318.29 | -66.0222 | 1318.13 | 33.3076 | 1318.13 | 34.96796 | 1318.13 | 38.72249 | 1318.13 | 61.11156 | 1318.13 | -39.1966 |  | 1318.13 | 45.07511 |
| 1318.47 | -4.06379 | 1318.96 | -66.0175 | 1318.8 | 32.48749 | 1318.8 | 33.10102 | 1318.8 | 37.18485 | 1318.8 | 59.37129 | 1318.8 | -40.4962 |  | 1318.8 | 44.39361 |
| 1319.14 | -4.02203 | 1319.63 | -66.9466 | 1319.47 | 32.53068 | 1319.47 | 31.06624 | 1319.47 | 36.07716 | 1319.47 | 57.46317 | 1319.47 | -41.3659 |  | 1319.47 | 44.57542 |
| 1319.81 | -3.98158 | 1320.29 | -67.428 | 1320.14 | 30.42288 | 1320.14 | 30.44805 | 1320.14 | 34.00852 | 1320.14 | 56.97165 | 1320.14 | -43.1966 |  | 1320.14 | 42.60623 |
| 1320.47 | -3.94222 | 1320.96 | -67.5944 | 1320.8 | 31.46126 | 1320.8 | 28.86438 | 1320.8 | 31.62976 | 1320.8 | 55.51275 | 1320.8 | -45.3409 |  | 1320.8 | 43.78115 |
| 1321.14 | -3.90402 | 1321.63 | -66.2234 | 1321.47 | 30.81638 | 1321.47 | 27.05381 | 1321.47 | 30.75043 | 1321.47 | 53.82885 | 1321.47 | -45.9822 |  | 1321.47 | 43.27487 |
| 1321.8 | -3.86721 | 1322.29 | -64.5749 | 1322.13 | 30.27373 | 1322.13 | 27.26833 | 1322.13 | 30.13264 | 1322.13 | 54.16815 | 1322.13 | -46.3656 |  | 1322.13 | 42.86877 |
| 1322.47 | -3.8319 | 1322.96 | -63.1415 | 1322.8 | 29.68605 | 1322.8 | 25.93636 | 1322.8 | 30.24779 | 1322.8 | 52.96285 | 1322.8 | -46.0124 |  | 1322.8 | 42.4197 |
| 1323.13 | -3.79817 | 1323.63 | -63.0826 | 1323.47 | 29.45874 | 1323.47 | 25.58346 | 1323.47 | 29.46624 | 1323.47 | 52.73662 | 1323.47 | -46.556 |  | 1323.47 | 42.331 |
| 1323.8 | -3.76603 | 1324.29 | -63.2561 | 1324.13 | 28.90192 | 1324.13 | 26.54628 | 1324.13 | 28.60375 | 1324.13 | 53.82421 | 1324.13 | -47.184 |  | 1324.13 | 41.91072 |
| 1324.46 | -3.73585 | 1324.96 | -62.9297 | 1324.8 | 29.92929 | 1324.8 | 25.95754 | 1324.8 | 29.66797 | 1324.8 | 53.36214 | 1324.8 | -45.8818 |  | 1324.8 | 43.0767 |
| 1325.13 | -3.70763 | 1325.62 | -62.291 | 1325.47 | 30.55919 | 1325.47 | 26.6536 | 1325.47 | 29.00613 | 1325.47 | 54.18487 | 1325.47 | -46.3056 |  | 1325.47 | 43.84521 |
| 1325.79 | -3.68143 | 1326.29 | -63.5599 | 1326.13 | 29.26839 | 1326.13 | 26.35848 | 1326.13 | 29.76408 | 1326.13 | 54.01452 | 1326.13 | -45.3132 |  | 1326.13 | 42.69095 |
| 1326.46 | -3.65729 | 1326.95 | -62.6361 | 1326.8 | 29.02864 | 1326.8 | 26.76235 | 1326.8 | 29.08399 | 1326.8 | 54.54505 | 1326.8 | -45.7553 |  | 1326.8 | 42.58981 |
| 1327.12 | -3.63503 | 1327.62 | -61.3507 | 1327.47 | 27.03671 | 1327.47 | 26.13941 | 1327.47 | 30.19543 | 1327.47 | 54.04878 | 1327.47 | -44.4059 |  | 1327.47 | 40.73649 |
| 1327.79 | -3.61451 | 1328.29 | -62.328 | 1328.13 | 25.7688 | 1328.13 | 26.64991 | 1328.13 | 28.24369 | 1328.13 | 54.68406 | 1328.13 | -46.1232 |  | 1328.13 | 39.60512 |
| 1328.45 | -3.59584 | 1328.95 | -63.4126 | 1328.8 | 24.82292 | 1328.8 | 25.67191 | 1328.8 | 26.73325 | 1328.8 | 53.83273 | 1328.8 | -47.3956 |  | 1328.8 | 38.79785 |
| 1329.12 | -3.57897 | 1329.62 | -64.5879 | 1329.46 | 23.09655 | 1329.46 | 24.46159 | 1329.46 | 25.5509 | 1329.46 | 52.74718 | 1329.46 | -48.3435 |  | 1329.46 | 37.20802 |
| 1329.78 | -3.56385 | 1330.28 | -63.6146 | 1330.13 | 21.13063 | 1330.13 | 22.7483 | 1330.13 | 23.80229 | 1330.13 | 51.16057 | 1330.13 | -49.8542 |  | 1330.13 | 35.38071 |
| 1330.44 | -3.55063 | 1330.95 | -63.6266 | 1330.8 | 19.8349 | 1330.8 | 22.13593 | 1330.8 | 22.49334 | 1330.8 | 50.67486 | 1330.8 | -50.9251 |  | 1330.8 | 34.22359 |
| 1331.11 | -3.53916 | 1331.61 | -62.5715 | 1331.46 | 18.85868 | 1331.46 | 21.7534 | 1331.46 | 21.47033 | 1331.46 | 50.41711 | 1331.46 | -51.7137 |  | 1331.46 | 33.38391 |
| 1331.77 | -3.529 | 1332.28 | -61.7873 | 1332.13 | 18.81604 | 1332.13 | 20.66354 | 1332.13 | 18.70038 | 1332.13 | 49.45391 | 1332.13 | -54.2456 |  | 1332.13 | 33.47989 |
| 1332.44 | -3.52036 | 1332.94 | -62.2251 | 1332.79 | 16.72664 | 1332.79 | 21.44861 | 1332.79 | 18.56696 | 1332.79 | 50.36376 | 1332.79 | -54.1446 |  | 1332.79 | 31.52702 |
| 1333.1 | -3.51349 | 1333.61 | -61.0976 | 1333.46 | 14.05987 | 1333.46 | 20.53707 | 1333.46 | 17.00542 | 1333.46 | 49.57889 | 1333.46 | -55.4681 |  | 1333.46 | 28.99886 |
| 1333.77 | -3.50843 | 1334.27 | -59.6793 | 1334.12 | 13.58358 | 1334.12 | 19.88572 | 1334.12 | 14.26738 | 1334.12 | 49.05231 | 1334.12 | -57.9717 |  | 1334.12 | 28.65911 |
| 1334.43 | -3.50483 | 1334.94 | -60.4449 | 1334.79 | 12.27461 | 1334.79 | 18.47669 | 1334.79 | 12.11072 | 1334.79 | 47.76995 | 1334.79 | -59.8904 |  | 1334.79 | 27.48875 |
| 1335.09 | -3.50278 | 1335.6 | -59.1505 | 1335.45 | 12.48771 | 1335.45 | 18.30659 | 1335.45 | 10.07971 | 1335.45 | 47.72463 | 1335.45 | -61.687 |  | 1335.45 | 27.8384 |
| 1335.76 | -3.50228 | 1336.27 | -58.6654 | 1336.12 | 12.31441 | 1336.12 | 17.67329 | 1336.12 | 9.44647 | 1336.12 | 47.21799 | 1336.12 | -62.0822 |  | 1336.12 | 27.8037 |
| 1336.42 | -3.50326 | 1336.93 | -57.9026 | 1336.78 | 12.63413 | 1336.78 | 17.70315 | 1336.78 | 7.76544 | 1336.78 | 47.37263 | 1336.78 | -63.5288 |  | 1336.78 | 28.25997 |
| 1337.09 | -3.50551 | 1337.6 | -59.5883 | 1337.45 | 13.52921 | 1337.45 | 18.37804 | 1337.45 | 7.25434 | 1337.45 | 48.17419 | 1337.45 | -63.8019 |  | 1337.45 | 29.29366 |
| 1337.75 | -3.50909 | 1338.26 | -60.1692 | 1338.11 | 12.6793 | 1338.11 | 16.98402 | 1338.11 | 4.97713 | 1338.11 | 46.90495 | 1338.11 | -65.8447 |  | 1338.11 | 28.58029 |
| 1338.41 | -3.51384 | 1338.93 | -61.0114 | 1338.78 | 11.84417 | 1338.78 | 16.33469 | 1338.78 | 3.86286 | 1338.78 | 46.38228 | 1338.78 | -66.7209 |  | 1338.78 | 27.88377 |
| 1339.08 | -3.51967 | 1339.59 | -61.1799 | 1339.44 | 11.97698 | 1339.44 | 15.47972 | 1339.44 | 2.94658 | 1339.44 | 45.65209 | 1339.44 | -67.4028 |  | 1339.44 | 28.15312 |
| 1339.74 | -3.52703 | 1340.26 | -60.4567 | 1340.11 | 11.21242 | 1340.11 | 15.49062 | 1340.11 | 4.49858 | 1340.11 | 45.78966 | 1340.11 | -65.6128 |  | 1340.11 | 27.52716 |
| 1340.4 | -3.53581 | 1340.92 | -60.0856 | 1340.77 | 10.67029 | 1340.77 | 14.09998 | 1340.77 | 5.3156 | 1340.77 | 44.5238 | 1340.77 | -64.5613 |  | 1340.77 | 27.12158 |
| 1341.07 | -3.54604 | 1341.59 | -60.5414 | 1341.44 | 9.41414 | 1341.44 | 13.14939 | 1341.44 | 2.76004 | 1341.44 | 43.69988 | 1341.44 | -66.8789 |  | 1341.44 | 26.00404 |
| 1341.73 | -3.5576 | 1342.25 | -59.0334 | 1342.1 | 7.23101 | 1342.1 | 11.8084 | 1342.1 | 1.51097 | 1342.1 | 42.48366 | 1342.1 | -67.8935 |  | 1342.1 | 23.95745 |
| 1342.39 | -3.57061 | 1342.91 | -60.8278 | 1342.77 | 6.10286 | 1342.77 | 10.91974 | 1342.77 | 0 | 1342.77 | 41.72166 | 1342.77 | -69.1665 |  | 1342.77 | 22.9679 |
| 1343.06 | -3.58517 | 1343.58 | -60.5452 | 1343.43 | 4.42108 | 1343.43 | 8.48432 | 1343.43 | 2.03487 | 1343.43 | 39.41102 | 1343.43 | -67.8716 |  | 1343.43 | 21.42267 |
| 1343.72 | -3.60139 | 1344.24 | -61.3631 | 1344.1 | 4.08918 | 1344.1 | 6.67216 | 1344.1 | 3.12369 | 1344.1 | 37.72553 | 1344.1 | -67.534 |  | 1344.1 | 21.22937 |
| 1344.38 | -3.61916 | 1344.91 | -60.0722 | 1344.76 | 2.13559 | 1344.76 | 5.97141 | 1344.76 | 2.00433 | 1344.76 | 37.14956 | 1344.76 | -69.3933 |  | 1344.76 | 19.41233 |
| 1345.05 | -3.63862 | 1345.57 | -59.0539 | 1345.43 | 0.40995 | 1345.43 | 6.00875 | 1345.43 | 2.36303 | 1345.43 | 37.31357 | 1345.43 | -69.7859 |  | 1345.43 | 17.8253 |
| 1345.71 | -3.65997 | 1346.23 | -58.8568 | 1346.09 | 0.53792 | 1346.09 | 4.36436 | 1346.09 | 1.16453 | 1346.09 | 35.79395 | 1346.09 | -71.7244 |  | 1346.09 | 18.08981 |
| 1346.37 | -3.68336 | 1346.9 | -58.7746 | 1346.75 | 0 | 1346.75 | 3.17657 | 1346.75 | 1.76771 | 1346.75 | 34.73094 | 1346.75 | -71.8612 |  | 1346.75 | 17.68843 |
| 1347.04 | -3.70859 | 1347.56 | -60.0774 | 1347.42 | -0.41479 | 1347.42 | 1.71229 | 1347.42 | 3.12611 | 1347.42 | 33.39333 | 1347.42 | -71.254 |  | 1347.42 | 17.25197 |
| 1347.7 | -3.7357 | 1348.23 | -61.8636 | 1348.08 | -1.80832 | 1348.08 | 0 | 1348.08 | 4.3718 | 1348.08 | 31.80581 | 1348.08 | -70.7483 |  | 1348.08 | 15.83708 |
| 1348.36 | -3.7646 | 1348.89 | -62.5393 | 1348.75 | -1.39387 | 1348.75 | 0.21378 | 1348.75 | 4.29655 | 1348.75 | 31.3677 | 1348.75 | -71.5748 |  | 1348.75 | 16.22984 |
| 1349.02 | -3.79568 | 1349.55 | -64.9543 | 1349.41 | -2.35368 | 1349.41 | -0.37525 | 1349.41 | 3.21832 | 1349.41 | 30.1365 | 1349.41 | -73.393 |  | 1349.41 | 15.24868 |
| 1349.36 | -3.82913 | 1350.22 | -64.5849 | 1350.07 | -2.97564 | 1350.07 | 0.30982 | 1350.07 | 2.79499 | 1350.07 | 30.1794 | 1350.07 | -74.5563 |  | 1350.07 | 14.60536 |
| 1350.03 | -3.86458 | 1350.88 | -65.1313 | 1350.74 | -1.9104 | 1350.74 | -2.56626 | 1350.74 | 2.69335 | 1350.74 | 26.65142 | 1350.74 | -75.4092 |  | 1350.74 | 15.64892 |
| 1350.69 | -3.9021 | 1351.54 | -66.4935 | 1351.4 | -2.10118 | 1351.4 | -2.58875 | 1351.4 | 1.80481 | 1351.4 | 25.98676 | 1351.4 | -77.0377 |  | 1351.4 | 15.43679 |
| 1351.36 | -3.94159 | 1352.21 | -67.887 | 1352.06 | -1.85664 | 1352.06 | -3.44683 | 1352.06 | 0.64262 | 1352.06 | 24.48651 | 1352.06 | -78.9399 |  | 1352.06 | 15.65997 |
| 1352.02 | -3.98283 | 1352.87 | -68.3238 | 1352.73 | 0.10369 | 1352.73 | -2.95661 | 1352.73 | 2.01294 | 1352.73 | 24.32483 | 1352.73 | -78.3208 |  | 1352.73 | 17.59863 |
| 1352.69 | -4.02594 | 1353.53 | -68.2321 | 1353.39 | -0.36079 | 1353.39 | -2.48191 | 1353.39 | 1.09193 | 1353.39 | 24.15737 | 1353.39 | -79.9818 |  | 1353.39 | 17.11278 |
| 1353.35 | -4.07107 | 1354.2 | -68.3628 | 1354.06 | 1.02191 | 1354.06 | -3.24239 | 1354.06 | 3.17644 | 1354.06 | 22.74499 | 1354.06 | -78.6485 |  | 1354.06 | 18.4738 |
| 1354.01 | -4.11752 | 1354.86 | -66.5826 | 1354.72 | 0.05978 | 1354.72 | -1.44015 | 1354.72 | 5.21316 | 1354.72 | 23.90506 | 1354.72 | -77.3518 |  | 1354.72 | 17.49033 |
| 1354.68 | -4.16523 | 1355.52 | -65.724 | 1355.38 | 0.4757 | 1355.38 | -1.09025 | 1355.38 | 3.65007 | 1355.38 | 23.61278 | 1355.38 | -79.6548 |  | 1355.38 | 17.88489 |
| 1355.34 | -4.21402 | 1356.19 | -65.9272 | 1356.05 | 0.51882 | 1356.05 | -2.45647 | 1356.05 | 1.57239 | 1356.05 | 21.59467 | 1356.05 | -82.4837 |  | 1356.05 | 17.90632 |
| 1356.01 | -4.26345 | 1356.85 | -66.0253 | 1356.71 | 1.06611 | 1356.71 | -1.36285 | 1356.71 | 1.85597 | 1356.71 | 22.04612 | 1356.71 | -82.9402 |  | 1356.71 | 18.43226 |
| 1356.67 | -4.3136 | 1357.51 | -65.3356 | 1357.37 | -0.04698 | 1357.37 | -1.57585 | 1357.37 | 1.17315 | 1357.37 | 21.19095 | 1357.37 | -84.363 |  | 1357.37 | 17.29781 |
| 1357.33 | -4.36463 | 1358.17 | -65.4663 | 1358.03 | -0.64439 | 1358.03 | -1.22395 | 1358.03 | 0.28112 | 1358.03 | 20.90069 | 1358.03 | -85.995 |  | 1358.03 | 16.67905 |
| 1358 | -4.41663 | 1358.84 | -63.9311 | 1358.7 | -1.51008 | 1358.7 | -2.07697 | 1358.7 | -1.64373 | 1358.7 | 19.39576 | 1358.7 | -88.6711 |  | 1358.7 | 15.79167 |
| 1358.66 | -4.46973 | 1359.5 | -64.2515 | 1359.36 | -1.15258 | 1359.36 | -2.51835 | 1359.36 | -2.78019 | 1359.36 | 18.31221 | 1359.36 | -90.5475 |  | 1359.36 | 16.12783 |
| 1359.32 | -4.52397 | 1360.16 | -64.5292 | 1360.02 | 0.28181 | 1360.02 | -2.54635 | 1360.02 | -4.35618 | 1360.02 | 17.64205 | 1360.02 | -92.8635 |  | 1360.02 | 17.54085 |
| 1359.99 | -4.57957 | 1360.82 | -63.5946 | 1360.69 | 0.57024 | 1360.69 | -2.86344 | 1360.69 | -4.519 | 1360.69 | 16.67306 | 1360.69 | -93.7775 |  | 1360.69 | 17.80761 |
| 1360.65 | -4.6366 | 1361.49 | -64.2504 | 1361.35 | 0.50364 | 1361.35 | -1.85791 | 1361.35 | -5.75812 | 1361.35 | 17.03642 | 1361.35 | -95.7567 |  | 1361.35 | 17.71965 |
| 1361.31 | -4.695 | 1362.15 | -66.7786 | 1362.01 | 0.99881 | 1362.01 | -3.02806 | 1362.01 | -8.4745 | 1362.01 | 15.2241 | 1362.01 | -99.213 |  | 1362.01 | 18.19347 |
| 1361.98 | -4.75439 | 1362.81 | -66.3656 | 1362.67 | 0.48046 | 1362.67 | -3.4466 | 1362.67 | -9.28257 | 1362.67 | 14.16339 | 1362.67 | -100.761 |  | 1362.67 | 17.65376 |
| 1362.64 | -4.81483 | 1363.47 | -67.6118 | 1363.34 | 0.30577 | 1363.34 | -3.47521 | 1363.34 | -10.7804 | 1363.34 | 13.48288 | 1363.34 | -103.01 |  | 1363.34 | 17.45739 |
| 1363.3 | -4.87604 | 1364.13 | -66.3012 | 1364 | 1.12134 | 1364 | -2.0312 | 1364 | -12.2997 | 1364 | 14.28473 | 1364 | -105.269 |  | 1364 | 18.2516 |
| 1363.97 | -4.93774 | 1364.8 | -65.9282 | 1364.66 | 1.33751 | 1364.66 | -2.29341 | 1364.66 | -11.6723 | 1364.66 | 13.38035 | 1364.66 | -105.382 |  | 1364.66 | 18.44642 |
| 1364.63 | -4.99979 | 1365.46 | -66.6819 | 1365.32 | 0.56271 | 1365.32 | -3.25052 | 1365.32 | -12.2743 | 1365.32 | 11.78107 | 1365.32 | -106.724 |  | 1365.32 | 17.65026 |
| 1365.29 | -5.06202 | 1366.12 | -67.6214 | 1365.99 | -0.17255 | 1365.99 | -2.89962 | 1365.99 | -12.1933 | 1365.99 | 11.48007 | 1365.99 | -107.394 |  | 1365.99 | 16.89332 |
| 1365.96 | -5.12421 | 1366.78 | -68.3551 | 1366.65 | 0.34991 | 1366.65 | -4.2659 | 1366.65 | -14.9538 | 1366.65 | 9.47162 | 1366.65 | -110.895 |  | 1366.65 | 17.39442 |
| 1366.62 | -5.18647 | 1367.44 | -67.8249 | 1367.31 | -0.3196 | 1367.31 | -3.88492 | 1367.31 | -15.7107 | 1367.31 | 9.21043 | 1367.31 | -112.392 |  | 1367.31 | 16.70356 |
| 1367.28 | -5.24889 | 1368.11 | -68.3099 | 1367.97 | 0.23719 | 1367.97 | -3.1735 | 1367.97 | -14.7042 | 1367.97 | 9.27968 | 1367.97 | -112.125 |  | 1367.97 | 17.23899 |
| 1367.94 | -5.31149 | 1368.77 | -68.5969 | 1368.63 | -0.07426 | 1368.63 | -1.7111 | 1368.63 | -12.9683 | 1368.63 | 10.09991 | 1368.63 | -111.129 |  | 1368.63 | 16.90618 |
| 1368.61 | -5.37403 | 1369.43 | -68.3989 | 1369.3 | -1.04971 | 1369.3 | -1.94505 | 1369.3 | -13.5034 | 1369.3 | 9.21406 | 1369.3 | -112.415 |  | 1369.3 | 15.90906 |
| 1369.27 | -5.43661 | 1370.09 | -68.519 | 1369.96 | -1.23879 | 1369.96 | -2.1777 | 1369.96 | -14.1313 | 1369.96 | 8.33924 | 1369.96 | -113.783 |  | 1369.96 | 15.69862 |
| 1369.93 | -5.49923 | 1370.75 | -68.0642 | 1370.62 | -1.72259 | 1370.62 | -3.00702 | 1370.62 | -14.8459 | 1370.62 | 6.86776 | 1370.62 | -115.238 |  | 1370.62 | 15.19347 |
| 1370.59 | -5.56188 | 1371.41 | -69.1709 | 1371.28 | -2.5456 | 1371.28 | -4.543 | 1371.28 | -16.2223 | 1371.28 | 4.68961 | 1371.28 | -117.354 |  | 1371.28 | 14.3491 |
| 1371.26 | -5.62453 | 1372.07 | -69.4639 | 1371.94 | -2.78702 | 1371.94 | -3.5007 | 1371.94 | -15.9258 | 1371.94 | 5.08974 | 1371.94 | -117.798 |  | 1371.94 | 14.08632 |
| 1371.92 | -5.68711 | 1372.74 | -67.6209 | 1372.6 | -2.77337 | 1372.6 | -3.07825 | 1372.6 | -16.2499 | 1372.6 | 4.87002 | 1372.6 | -118.862 |  | 1372.6 | 14.07862 |
| 1372.58 | -5.74966 | 1373.4 | -67.3532 | 1373.27 | -2.83701 | 1373.27 | -2.64224 | 1373.27 | -16.6988 | 1373.27 | 4.65413 | 1373.27 | -120.062 |  | 1373.27 | 13.9933 |
| 1373.24 | -5.81194 | 1374.06 | -66.5138 | 1373.93 | -2.82922 | 1373.93 | -2.42131 | 1373.93 | -19.1639 | 1373.93 | 4.23289 | 1373.93 | -123.267 |  | 1373.93 | 13.97973 |
| 1373.91 | -5.8742 | 1374.72 | -66.5496 | 1374.59 | -2.98691 | 1374.59 | -1.38739 | 1374.59 | -20.226 | 1374.59 | 4.62464 | 1374.59 | -125.069 |  | 1374.59 | 13.80068 |
| 1374.57 | -5.9365 | 1375.38 | -68.1304 | 1375.25 | -2.46911 | 1375.25 | -0.08857 | 1375.25 | -16.9969 | 1375.25 | 5.28129 | 1375.25 | -122.58 |  | 1375.25 | 14.29713 |
| 1375.23 | -5.9985 | 1376.04 | -68.3555 | 1375.91 | -0.77091 | 1375.91 | 0.22247 | 1375.91 | -17.5707 | 1375.91 | 5.25271 | 1375.91 | -123.894 |  | 1375.91 | 15.97397 |
| 1375.89 | -6.05996 | 1376.7 | -67.5761 | 1376.57 | 0.13063 | 1376.57 | 0.1509 | 1376.57 | -16.76 | 1376.57 | 4.89255 | 1376.57 | -123.823 |  | 1376.57 | 16.85415 |
| 1376.55 | -6.12109 | 1377.36 | -67.7856 | 1377.23 | 1.48255 | 1377.23 | 1.49326 | 1377.23 | -16.2314 | 1377.23 | 5.94631 | 1377.23 | -124.035 |  | 1377.23 | 18.18473 |
| 1377.22 | -6.18187 | 1378.02 | -67.62 | 1377.9 | 1.96639 | 1377.9 | 2.85905 | 1377.9 | -16.913 | 1377.9 | 7.01914 | 1377.9 | -125.467 |  | 1377.9 | 18.64688 |
| 1377.88 | -6.24195 | 1378.69 | -68.4204 | 1378.56 | 3.76244 | 1378.56 | 3.78499 | 1378.56 | -15.3733 | 1378.56 | 7.65649 | 1378.56 | -124.668 |  | 1378.56 | 20.42158 |
| 1378.54 | -6.30141 | 1379.35 | -68.9567 | 1379.22 | 6.06144 | 1379.22 | 4.07092 | 1379.22 | -14.429 | 1379.22 | 7.65383 | 1379.22 | -124.464 |  | 1379.22 | 22.69922 |
| 1379.2 | -6.36026 | 1380.01 | -69.4682 | 1379.88 | 7.08691 | 1379.88 | 5.68921 | 1379.88 | -12.447 | 1379.88 | 8.98353 | 1379.88 | -123.222 |  | 1379.88 | 23.70334 |
| 1379.86 | -6.41835 | 1380.67 | -69.2569 | 1380.54 | 6.79494 | 1380.54 | 6.09735 | 1380.54 | -11.682 | 1380.54 | 9.10308 | 1380.54 | -123.197 |  | 1380.54 | 23.39001 |
| 1380.52 | -6.47577 | 1381.33 | -68.0312 | 1381.2 | 7.89689 | 1381.2 | 7.52667 | 1381.2 | -11.5602 | 1381.2 | 10.2438 | 1381.2 | -123.815 |  | 1381.2 | 24.47061 |
| 1381.18 | -6.53214 | 1381.99 | -68.1663 | 1381.86 | 9.21826 | 1381.86 | 7.51579 | 1381.86 | -11.1606 | 1381.86 | 9.94434 | 1381.86 | -124.155 |  | 1381.86 | 25.77061 |
| 1381.85 | -6.58753 | 1382.65 | -67.8356 | 1382.52 | 9.65884 | 1382.52 | 8.7253 | 1382.52 | -9.75976 | 1382.52 | 10.86526 | 1382.52 | -123.494 |  | 1382.52 | 26.18984 |
| 1382.51 | -6.64197 | 1383.31 | -67.4095 | 1383.18 | 11.00766 | 1383.18 | 9.48565 | 1383.18 | -8.56959 | 1383.18 | 11.33702 | 1383.18 | -123.044 |  | 1383.18 | 27.51731 |
| 1383.17 | -6.69548 | 1383.97 | -66.8694 | 1383.84 | 12.97904 | 1383.84 | 10.08639 | 1383.84 | -6.59098 | 1383.84 | 11.64916 | 1383.84 | -121.805 |  | 1383.84 | 29.46732 |
| 1383.83 | -6.7481 | 1384.63 | -66.7866 | 1384.5 | 13.30729 | 1384.5 | 11.32973 | 1384.5 | -6.00582 | 1384.5 | 12.60391 | 1384.5 | -121.96 |  | 1384.5 | 29.77422 |
| 1384.49 | -6.79929 | 1385.29 | -65.1116 | 1385.16 | 14.32201 | 1385.16 | 12.33581 | 1385.16 | -5.22615 | 1385.16 | 13.32141 | 1385.16 | -121.921 |  | 1385.16 | 30.76758 |
| 1385.15 | -6.84916 | 1385.95 | -64.1606 | 1385.82 | 15.38398 | 1385.82 | 13.12013 | 1385.82 | -4.84002 | 1385.82 | 13.81714 | 1385.82 | -122.275 |  | 1385.82 | 31.8082 |
| 1385.81 | -6.89759 | 1386.61 | -63.8928 | 1386.48 | 14.60832 | 1386.48 | 13.16783 | 1386.48 | -4.34615 | 1386.48 | 13.57625 | 1386.48 | -122.521 |  | 1386.48 | 31.01119 |
| 1386.47 | -6.94439 | 1387.27 | -63.7043 | 1387.14 | 14.77148 | 1387.14 | 14.33632 | 1387.14 | -3.03111 | 1387.14 | 14.45614 | 1387.14 | -121.946 |  | 1387.14 | 31.15299 |
| 1387.13 | -6.98958 | 1387.93 | -63.9577 | 1387.81 | 15.87046 | 1387.81 | 15.68839 | 1387.81 | -3.22055 | 1387.81 | 15.51526 | 1387.81 | -122.886 |  | 1387.81 | 32.23029 |
| 1387.8 | -7.03316 | 1388.59 | -64.7751 | 1388.46 | 16.64565 | 1388.46 | 15.16055 | 1388.46 | -3.50162 | 1388.46 | 14.70319 | 1388.46 | -123.896 |  | 1388.46 | 32.98445 |
| 1388.46 | -7.07515 | 1389.25 | -64.3532 | 1389.13 | 18.04327 | 1389.13 | 16.77777 | 1389.13 | -1.80176 | 1389.13 | 16.02745 | 1389.13 | -122.947 |  | 1389.13 | 34.36039 |
| 1389.12 | -7.11552 | 1389.91 | -64.4936 | 1389.78 | 19.43769 | 1389.78 | 17.48605 | 1389.78 | 0.45489 | 1389.78 | 16.45152 | 1389.78 | -121.42 |  | 1389.78 | 35.73377 |
| 1389.78 | -7.15403 | 1390.57 | -64.2339 | 1390.45 | 20.93532 | 1390.45 | 17.64294 | 1390.45 | -0.28811 | 1390.45 | 16.31544 | 1390.45 | -122.914 |  | 1390.45 | 37.20972 |
| 1390.44 | -7.19074 | 1391.23 | -64.5438 | 1391.1 | 23.17053 | 1391.1 | 17.0446 | 1391.1 | 0.13117 | 1391.1 | 15.43288 | 1391.1 | -123.223 |  | 1391.1 | 39.42391 |
| 1391.1 | -7.22556 | 1391.89 | -63.7446 | 1391.76 | 23.89862 | 1391.76 | 17.1028 | 1391.76 | -0.26579 | 1391.76 | 15.20249 | 1391.76 | -124.36 |  | 1391.76 | 40.13064 |
| 1391.76 | -7.25875 | 1392.55 | -64.6674 | 1392.42 | 24.42103 | 1392.42 | 17.88001 | 1392.42 | -0.28882 | 1392.42 | 15.69111 | 1392.42 | -125.123 |  | 1392.42 | 40.63168 |
| 1392.42 | -7.29039 | 1393.2 | -64.4455 | 1393.08 | 23.54344 | 1393.08 | 18.54453 | 1393.08 | -0.10836 | 1393.08 | 16.06704 | 1393.08 | -125.408 |  | 1393.08 | 39.73274 |
| 1393.08 | -7.32047 | 1393.86 | -64.2467 | 1393.74 | 23.00899 | 1393.74 | 19.39199 | 1393.74 | 0.38663 | 1393.74 | 16.62591 | 1393.74 | -124.902 |  | 1393.74 | 39.17694 |
| 1393.74 | -7.34909 | 1394.52 | -64.921 | 1394.4 | 24.08003 | 1394.4 | 21.52102 | 1394.4 | -0.03604 | 1394.4 | 18.46635 | 1394.4 | -125.313 |  | 1394.4 | 40.22662 |
| 1394.4 | -7.3765 | 1395.18 | -64.1638 | 1395.06 | 24.90305 | 1395.06 | 22.37422 | 1395.06 | 1.09725 | 1395.06 | 19.03096 | 1395.06 | -124.168 |  | 1395.06 | 41.02828 |
| 1395.06 | -7.4028 | 1395.84 | -64.8917 | 1395.72 | 25.48352 | 1395.72 | 24.3406 | 1395.72 | 2.74808 | 1395.72 | 20.70875 | 1395.72 | -122.505 |  | 1395.72 | 41.5874 |
| 1395.72 | -7.42788 | 1396.5 | -66.2496 | 1396.38 | 25.67714 | 1396.38 | 24.99424 | 1396.38 | 4.84695 | 1396.38 | 21.0738 | 1396.38 | -120.395 |  | 1396.38 | 41.75966 |
| 1396.38 | -7.45129 | 1397.16 | -65.296 | 1397.04 | 26.10251 | 1397.04 | 25.93769 | 1397.04 | 4.97542 | 1397.04 | 21.72866 | 1397.04 | -120.254 |  | 1397.04 | 42.16368 |
| 1397.04 | -7.47289 | 1397.82 | -64.6667 | 1397.7 | 26.95946 | 1397.7 | 26.85799 | 1397.7 | 5.01095 | 1397.7 | 22.36037 | 1397.7 | -120.207 |  | 1397.7 | 42.99927 |
| 1397.7 | -7.49265 | 1398.48 | -64.0882 | 1398.36 | 26.9127 | 1398.36 | 26.56325 | 1398.36 | 4.55695 | 1398.36 | 21.77704 | 1398.36 | -120.65 |  | 1398.36 | 42.93115 |
| 1398.36 | -7.51048 | 1399.14 | -65.1567 | 1399.02 | 28.26181 | 1399.02 | 28.80282 | 1399.02 | 5.16727 | 1399.02 | 23.72802 | 1399.02 | -120.028 |  | 1399.02 | 44.25891 |
| 1399.02 | -7.52621 | 1399.79 | -64.1829 | 1399.68 | 29.39897 | 1399.68 | 29.81926 | 1399.68 | 6.47621 | 1399.68 | 24.45587 | 1399.68 | -118.707 |  | 1399.68 | 45.37471 |
| 1399.68 | -7.53977 | 1400.45 | -63.2797 | 1400.34 | 30.69004 | 1400.34 | 31.99805 | 1400.34 | 8.39476 | 1400.34 | 26.34606 | 1400.34 | -116.777 |  | 1400.34 | 46.64443 |
| 1400.34 | -7.55129 | 1401.11 | -64.5424 | 1400.99 | 33.06198 | 1400.99 | 31.70937 | 1400.99 | 7.44573 | 1400.99 | 25.77317 | 1400.99 | -117.714 |  | 1400.99 | 48.99534 |
| 1401 | -7.56067 | 1401.77 | -64.4253 | 1401.65 | 33.08072 | 1401.65 | 31.92429 | 1401.65 | 8.77985 | 1401.65 | 25.6995 | 1401.65 | -116.368 |  | 1401.65 | 48.99272 |
| 1401.66 | -7.56795 | 1402.43 | -64.308 | 1402.31 | 35.11789 | 1402.31 | 32.13587 | 1402.31 | 8.37966 | 1402.31 | 25.62249 | 1402.31 | -116.757 |  | 1402.31 | 51.00853 |
| 1402.32 | -7.57319 | 1403.09 | -62.8208 | 1402.97 | 36.62937 | 1402.97 | 32.2955 | 1402.97 | 8.53005 | 1402.97 | 25.49352 | 1402.97 | -116.595 |  | 1402.97 | 52.49865 |
| 1402.97 | -7.57639 | 1403.74 | -61.0983 | 1403.63 | 37.54851 | 1403.63 | 32.51674 | 1403.63 | 7.79641 | 1403.63 | 25.42617 | 1403.63 | -117.317 |  | 1403.63 | 53.39644 |
| 1403.63 | -7.57763 | 1404.4 | -61.942 | 1404.29 | 38.31764 | 1404.29 | 33.94896 | 1404.29 | 7.44042 | 1404.29 | 26.56981 | 1404.29 | -117.661 |  | 1404.29 | 54.14422 |
| 1404.29 | -7.57684 | 1405.06 | -62.5386 | 1404.95 | 38.16876 | 1404.95 | 36.29162 | 1404.95 | 7.77018 | 1404.95 | 28.62388 | 1404.95 | -117.32 |  | 1404.95 | 53.97397 |
| 1404.95 | -7.57422 | 1405.72 | -63.2368 | 1405.6 | 39.06856 | 1405.6 | 37.41893 | 1405.6 | 8.02464 | 1405.6 | 29.46697 | 1405.6 | -117.054 |  | 1405.6 | 54.85275 |
| 1405.61 | -7.56988 | 1406.38 | -61.5872 | 1406.26 | 40.86792 | 1406.26 | 38.08988 | 1406.26 | 7.27822 | 1406.26 | 29.84933 | 1406.26 | -117.789 |  | 1406.26 | 56.63075 |
| 1406.27 | -7.5638 | 1407.03 | -62.0029 | 1406.92 | 41.40276 | 1406.92 | 39.16588 | 1406.92 | 7.43485 | 1406.92 | 30.63674 | 1406.92 | -117.62 |  | 1406.92 | 57.14423 |
| 1406.93 | -7.55593 | 1407.69 | -63.8464 | 1407.58 | 41.68978 | 1407.58 | 39.22668 | 1407.58 | 7.32517 | 1407.58 | 30.40895 | 1407.58 | -117.718 |  | 1407.58 | 57.40989 |
| 1407.59 | -7.54584 | 1408.35 | -63.3669 | 1408.24 | 41.67247 | 1408.24 | 40.96685 | 1408.24 | 8.49717 | 1408.24 | 31.86052 | 1408.24 | -116.535 |  | 1408.24 | 57.37123 |
| 1408.25 | -7.53378 | 1409.01 | -63.1845 | 1408.9 | 42.24065 | 1408.9 | 41.36956 | 1408.9 | 7.04192 | 1408.9 | 31.97465 | 1408.9 | -117.978 |  | 1408.9 | 57.91806 |
| 1408.91 | -7.51993 | 1409.67 | -62.9308 | 1409.55 | 42.09421 | 1409.55 | 42.11246 | 1409.55 | 6.96105 | 1409.55 | 32.43333 | 1409.55 | -118.048 |  | 1409.55 | 57.75058 |
| 1409.56 | -7.50432 | 1410.32 | -64.1279 | 1410.21 | 42.91907 | 1410.21 | 42.69307 | 1410.21 | 6.8596 | 1410.21 | 32.72535 | 1410.21 | -118.137 |  | 1410.21 | 58.55409 |
| 1410.22 | -7.48817 | 1410.98 | -65.5806 | 1410.87 | 43.5604 | 1410.87 | 42.37858 | 1410.87 | 6.686 | 1410.87 | 32.12227 | 1410.87 | -118.299 |  | 1410.87 | 59.17406 |
| 1410.88 | -7.47146 | 1411.64 | -64.7333 | 1411.53 | 42.95213 | 1411.53 | 42.62433 | 1411.53 | 5.92699 | 1411.53 | 32.07943 | 1411.53 | -119.047 |  | 1411.53 | 58.54444 |
| 1411.54 | -7.45412 | 1412.29 | -64.2599 | 1412.18 | 43.1008 | 1412.18 | 42.57571 | 1412.18 | 5.36129 | 1412.18 | 31.74659 | 1412.18 | -119.601 |  | 1412.18 | 58.67207 |
| 1412.2 | -7.43587 | 1412.95 | -64.838 | 1412.84 | 42.38804 | 1412.84 | 44.32975 | 1412.84 | 4.71295 | 1412.84 | 33.21204 | 1412.84 | -120.237 |  | 1412.84 | 57.93795 |
| 1412.86 | -7.41675 | 1413.61 | -66.6176 | 1413.5 | 41.87645 | 1413.5 | 45.04752 | 1413.5 | 5.27303 | 1413.5 | 33.64122 | 1413.5 | -119.666 |  | 1413.5 | 57.40501 |
| 1413.51 | -7.39693 | 1414.27 | -67.8962 | 1414.16 | 43.43231 | 1414.16 | 45.83038 | 1414.16 | 4.07763 | 1414.16 | 34.13549 | 1414.16 | -120.849 |  | 1414.16 | 58.93952 |
| 1414.17 | -7.37632 | 1414.92 | -67.6702 | 1414.81 | 44.00885 | 1414.81 | 46.7603 | 1414.81 | 5.73052 | 1414.81 | 34.78119 | 1414.81 | -119.185 |  | 1414.81 | 59.49502 |
| 1414.83 | -7.35473 | 1415.58 | -67.4835 | 1415.47 | 44.10747 | 1415.47 | 48.64027 | 1415.47 | 6.18873 | 1415.47 | 36.37257 | 1415.47 | -118.715 |  | 1415.47 | 59.57228 |
| 1415.49 | -7.33175 | 1416.24 | -67.6304 | 1416.13 | 44.09688 | 1416.13 | 50.36343 | 1416.13 | 6.49603 | 1416.13 | 37.80714 | 1416.13 | -118.396 |  | 1416.13 | 59.54035 |
| 1416.15 | -7.30744 | 1416.9 | -68.1282 | 1416.79 | 43.89787 | 1416.79 | 51.54091 | 1416.79 | 6.47647 | 1416.79 | 38.69603 | 1416.79 | -118.404 |  | 1416.79 | 59.31998 |
| 1416.8 | -7.28178 | 1417.55 | -67.5618 | 1417.44 | 42.16992 | 1417.44 | 52.44151 | 1417.44 | 6.50364 | 1417.44 | 39.31241 | 1417.44 | -118.365 |  | 1417.44 | 57.57099 |
| 1417.46 | -7.25448 | 1418.21 | -67.4436 | 1418.1 | 41.90875 | 1418.1 | 52.99879 | 1418.1 | 6.79976 | 1418.1 | 39.5811 | 1418.1 | -118.058 |  | 1418.1 | 57.28846 |
| 1418.12 | -7.22553 | 1418.87 | -68.1917 | 1418.76 | 41.61797 | 1418.76 | 55.10371 | 1418.76 | 6.2806 | 1418.76 | 41.39743 | 1418.76 | -118.565 |  | 1418.76 | 56.97633 |
| 1418.78 | -7.19445 | 1419.52 | -68.4106 | 1419.42 | 41.74955 | 1419.42 | 56.38496 | 1419.42 | 8.30151 | 1419.42 | 42.39009 | 1419.42 | -116.533 |  | 1419.42 | 57.08656 |
| 1419.43 | -7.16128 | 1420.18 | -67.0086 | 1420.07 | 41.8367 | 1420.07 | 58.15262 | 1420.07 | 7.94377 | 1420.07 | 43.87354 | 1420.07 | -116.879 |  | 1420.07 | 57.15267 |
| 1420.09 | -7.12601 | 1420.83 | -66.0735 | 1420.73 | 42.50261 | 1420.73 | 58.96549 | 1420.73 | 9.06751 | 1420.73 | 44.39781 | 1420.73 | -115.743 |  | 1420.73 | 57.79722 |
| 1420.75 | -7.08876 | 1421.49 | -65.0114 | 1421.39 | 41.66322 | 1421.39 | 59.65052 | 1421.39 | 9.67282 | 1421.39 | 44.79425 | 1421.39 | -115.126 |  | 1421.39 | 56.93648 |
| 1421.41 | -7.04951 | 1422.15 | -64.2765 | 1422.04 | 40.38196 | 1422.04 | 60.21847 | 1422.04 | 11.22132 | 1422.04 | 45.07799 | 1422.04 | -113.566 |  | 1422.04 | 55.63419 |
| 1422.07 | -7.0081 | 1422.81 | -63.6028 | 1422.7 | 40.61905 | 1422.7 | 59.93017 | 1422.7 | 12.52623 | 1422.7 | 44.50109 | 1422.7 | -112.25 |  | 1422.7 | 55.84992 |
| 1422.72 | -6.96433 | 1423.46 | -63.5266 | 1423.36 | 39.76066 | 1423.36 | 60.37308 | 1423.36 | 12.15397 | 1423.36 | 44.65542 | 1423.36 | -112.61 |  | 1423.36 | 54.97017 |
| 1423.38 | -6.91786 | 1424.12 | -63.3924 | 1424.01 | 38.37979 | 1424.01 | 61.66575 | 1424.01 | 13.75071 | 1424.01 | 45.66386 | 1424.01 | -111.002 |  | 1424.01 | 53.56827 |
| 1424.04 | -6.86848 | 1424.77 | -63.0256 | 1424.67 | 37.98847 | 1424.67 | 63.05872 | 1424.67 | 13.96087 | 1424.67 | 46.76824 | 1424.67 | -110.78 |  | 1424.67 | 53.15559 |
| 1424.69 | -6.81621 | 1425.43 | -62.6276 | 1425.33 | 37.39911 | 1425.33 | 64.27345 | 1425.33 | 16.61418 | 1425.33 | 47.69439 | 1425.33 | -108.115 |  | 1425.33 | 52.54488 |
| 1425.35 | -6.76085 | 1426.09 | -62.221 | 1425.98 | 37.50924 | 1425.98 | 65.68523 | 1425.98 | 18.92617 | 1425.98 | 48.82195 | 1425.98 | -105.792 |  | 1425.98 | 52.63398 |
| 1426.01 | -6.70243 | 1426.74 | -63.0818 | 1426.64 | 38.38753 | 1426.64 | 66.92369 | 1426.64 | 20.95928 | 1426.64 | 49.77182 | 1426.64 | -103.747 |  | 1426.64 | 53.49091 |
| 1426.66 | -6.64077 | 1427.4 | -64.1115 | 1427.3 | 38.62328 | 1427.3 | 68.50436 | 1427.3 | 24.73679 | 1427.3 | 51.0639 | 1427.3 | -99.9579 |  | 1427.3 | 53.7053 |
| 1427.32 | -6.57574 | 1428.05 | -64.3066 | 1427.95 | 37.22929 | 1427.95 | 69.10516 | 1427.95 | 26.19643 | 1427.95 | 51.38048 | 1427.95 | -98.4868 |  | 1427.95 | 52.29028 |
| 1427.98 | -6.50749 | 1428.71 | -63.9816 | 1428.61 | 36.77368 | 1428.61 | 69.19803 | 1428.61 | 27.10695 | 1428.61 | 51.18476 | 1428.61 | -97.5646 |  | 1428.61 | 51.81332 |
| 1428.64 | -6.43597 | 1429.36 | -63.6496 | 1429.26 | 35.72951 | 1429.26 | 70.01281 | 1429.26 | 27.70706 | 1429.26 | 51.71532 | 1429.26 | -96.953 |  | 1429.26 | 50.74811 |
| 1429.29 | -6.36079 | 1430.02 | -63.7219 | 1429.92 | 36.36331 | 1429.92 | 70.48352 | 1429.92 | 27.70896 | 1429.92 | 51.89745 | 1429.92 | -96.9394 |  | 1429.92 | 51.36056 |
| 1429.95 | -6.28177 | 1430.68 | -62.7219 | 1430.58 | 35.7832 | 1430.58 | 72.79821 | 1430.58 | 29.49976 | 1430.58 | 53.92354 | 1430.58 | -95.137 |  | 1430.58 | 50.75909 |
| 1430.61 | -6.19863 | 1431.33 | -62.5997 | 1431.23 | 34.69669 | 1431.23 | 73.99911 | 1431.23 | 32.55211 | 1431.23 | 54.84023 | 1431.23 | -92.0731 |  | 1431.23 | 49.65155 |
| 1431.26 | -6.11099 | 1431.99 | -62.6772 | 1431.89 | 34.63246 | 1431.89 | 76.76988 | 1431.89 | 35.40742 | 1431.89 | 57.3224 | 1431.89 | -89.2061 |  | 1431.89 | 49.56597 |
| 1431.92 | -6.01873 | 1432.64 | -62.5603 | 1432.54 | 34.6385 | 1432.54 | 77.57843 | 1432.54 | 37.27918 | 1432.54 | 57.84674 | 1432.54 | -87.3229 |  | 1432.54 | 49.55097 |
| 1432.57 | -5.92181 | 1433.3 | -62.5123 | 1433.2 | 34.01115 | 1433.2 | 78.46238 | 1433.2 | 37.67123 | 1433.2 | 58.4421 | 1433.2 | -86.9192 |  | 1433.2 | 48.90227 |
| 1433.23 | -5.82011 | 1433.95 | -62.0146 | 1433.85 | 32.58505 | 1433.85 | 78.62888 | 1433.85 | 38.6104 | 1433.85 | 58.32437 | 1433.85 | -85.9685 |  | 1433.85 | 47.45514 |
| 1433.89 | -5.71377 | 1434.61 | -62.5652 | 1434.51 | 31.9426 | 1434.51 | 80.49832 | 1434.51 | 40.51442 | 1434.51 | 59.90523 | 1434.51 | -84.0528 |  | 1434.51 | 46.79133 |
| 1434.54 | -5.60318 | 1435.26 | -63.3811 | 1435.17 | 32.52428 | 1435.17 | 81.45546 | 1435.17 | 40.4342 | 1435.17 | 60.57378 | 1435.17 | -84.1214 |  | 1435.17 | 47.35166 |
| 1435.2 | -5.48825 | 1435.92 | -63.6301 | 1435.82 | 32.63525 | 1435.82 | 81.51843 | 1435.82 | 41.39788 | 1435.82 | 60.35252 | 1435.82 | -83.1462 |  | 1435.82 | 47.44159 |
| 1435.86 | -5.36929 | 1436.57 | -62.7537 | 1436.48 | 32.50125 | 1436.48 | 83.22973 | 1436.48 | 43.26853 | 1436.48 | 61.77524 | 1436.48 | -81.2639 |  | 1436.48 | 47.28623 |
| 1436.51 | -5.24646 | 1437.23 | -61.8799 | 1437.13 | 32.35732 | 1437.13 | 86.39314 | 1437.13 | 45.26895 | 1437.13 | 64.65443 | 1437.13 | -79.2519 |  | 1437.13 | 47.12128 |
| 1437.17 | -5.12027 | 1437.88 | -63.1741 | 1437.79 | 32.39509 | 1437.79 | 87.42347 | 1437.79 | 47.28627 | 1437.79 | 65.39617 | 1437.79 | -77.223 |  | 1437.79 | 47.13769 |
| 1437.82 | -4.99097 | 1438.54 | -63.6787 | 1438.44 | 32.36922 | 1438.44 | 87.33967 | 1438.44 | 47.20834 | 1438.44 | 65.02815 | 1438.44 | -77.2894 |  | 1438.44 | 47.09078 |
| 1438.48 | -4.85869 | 1439.19 | -64.3863 | 1439.1 | 33.08131 | 1439.1 | 88.25652 | 1439.1 | 48.02063 | 1439.1 | 65.65641 | 1439.1 | -76.4654 |  | 1439.1 | 47.78152 |
| 1439.13 | -4.72399 | 1439.85 | -65.3973 | 1439.75 | 32.80936 | 1439.75 | 88.70507 | 1439.75 | 49.89114 | 1439.75 | 65.82075 | 1439.75 | -74.5834 |  | 1439.75 | 47.48853 |
| 1439.79 | -4.58717 | 1440.5 | -66.5903 | 1440.41 | 33.46009 | 1440.41 | 88.71923 | 1440.41 | 51.39724 | 1440.41 | 65.54631 | 1440.41 | -73.0656 |  | 1440.41 | 48.11791 |
| 1440.45 | -4.44864 | 1441.16 | -66.6254 | 1441.06 | 33.52599 | 1441.06 | 89.03411 | 1441.06 | 55.11194 | 1441.06 | 65.57697 | 1441.06 | -69.3394 |  | 1441.06 | 48.16278 |
| 1441.1 | -4.30846 | 1441.81 | -65.53 | 1441.72 | 34.10653 | 1441.72 | 90.06807 | 1441.72 | 55.86381 | 1441.72 | 66.32234 | 1441.72 | -68.5759 |  | 1441.72 | 48.72196 |
| 1441.76 | -4.16653 | 1442.47 | -64.6855 | 1442.37 | 32.85832 | 1442.37 | 90.22162 | 1442.37 | 56.51779 | 1442.37 | 66.19168 | 1442.37 | -67.9104 |  | 1442.37 | 47.45272 |
| 1442.41 | -4.02314 | 1443.12 | -64.7571 | 1443.03 | 32.52593 | 1443.03 | 90.37171 | 1443.03 | 57.88952 | 1443.03 | 66.05318 | 1443.03 | -66.527 |  | 1443.03 | 47.09897 |
| 1443.07 | -3.87846 | 1443.77 | -65.4702 | 1443.68 | 31.88224 | 1443.68 | 90.21742 | 1443.68 | 57.69348 | 1443.68 | 65.61467 | 1443.68 | -66.7116 |  | 1443.68 | 46.43425 |
| 1443.72 | -3.73293 | 1444.43 | -65.6777 | 1444.34 | 30.83319 | 1444.34 | 91.1105 | 1444.34 | 57.25644 | 1444.34 | 66.21916 | 1444.34 | -67.1369 |  | 1444.34 | 45.36384 |
| 1444.38 | -3.58656 | 1445.08 | -65.3519 | 1444.99 | 31.83166 | 1444.99 | 90.63783 | 1444.99 | 57.29339 | 1444.99 | 65.46227 | 1444.99 | -67.0885 |  | 1444.99 | 46.34128 |
| 1445.03 | -3.43901 | 1445.74 | -66.1183 | 1445.64 | 30.17976 | 1445.64 | 91.61306 | 1445.64 | 57.7607 | 1445.64 | 66.15328 | 1445.64 | -66.6097 |  | 1445.64 | 44.66834 |
| 1445.69 | -3.2903 | 1446.39 | -66.5518 | 1446.3 | 28.55345 | 1446.3 | 91.04084 | 1446.3 | 58.32882 | 1446.3 | 65.29247 | 1446.3 | -66.0299 |  | 1446.3 | 43.02069 |
| 1446.34 | -3.14051 | 1447.05 | -66.2966 | 1446.95 | 27.8388 | 1446.95 | 90.88842 | 1446.95 | 58.39905 | 1446.95 | 64.85584 | 1446.95 | -65.9482 |  | 1446.95 | 42.285 |
| 1447 | -2.98971 | 1447.7 | -65.7795 | 1447.61 | 26.98132 | 1447.61 | 90.59238 | 1447.61 | 58.4375 | 1447.61 | 64.27121 | 1447.61 | -65.8981 |  | 1447.61 | 41.40617 |
| 1447.65 | -2.83842 | 1448.35 | -65.5869 | 1448.26 | 26.11263 | 1448.26 | 90.17329 | 1448.26 | 56.46358 | 1448.26 | 63.5679 | 1448.26 | -67.8605 |  | 1448.26 | 40.51644 |
| 1448.31 | -2.68682 | 1449.01 | -66.1774 | 1448.92 | 25.42718 | 1448.92 | 89.15353 | 1448.92 | 55.44868 | 1448.92 | 62.25955 | 1448.92 | -68.8637 |  | 1448.92 | 39.80964 |
| 1448.96 | -2.53506 | 1449.66 | -66.4422 | 1449.57 | 25.36551 | 1449.57 | 87.82018 | 1449.57 | 54.43051 | 1449.57 | 60.64198 | 1449.57 | -69.8704 |  | 1449.57 | 39.72693 |
| 1449.62 | -2.3834 | 1450.31 | -67.0514 | 1450.22 | 24.57206 | 1450.22 | 87.4859 | 1450.22 | 54.7323 | 1450.22 | 60.02348 | 1450.22 | -69.5571 |  | 1450.22 | 38.91245 |
| 1450.27 | -2.23218 | 1450.97 | -68.0003 | 1450.88 | 24.83372 | 1450.88 | 87.36594 | 1450.88 | 53.65766 | 1450.88 | 59.61493 | 1450.88 | -70.6201 |  | 1450.88 | 39.15275 |
| 1450.93 | -2.08168 | 1451.62 | -68.4393 | 1451.53 | 23.74799 | 1451.53 | 87.46028 | 1451.53 | 53.02904 | 1451.53 | 59.42506 | 1451.53 | -71.2372 |  | 1451.53 | 38.04599 |
| 1451.58 | -1.932 | 1452.27 | -68.3957 | 1452.19 | 22.88787 | 1452.19 | 84.99199 | 1452.19 | 53.89629 | 1452.19 | 56.66818 | 1452.19 | -70.3583 |  | 1452.19 | 37.16451 |
| 1452.24 | -1.78342 | 1452.93 | -67.2844 | 1452.84 | 21.07523 | 1452.84 | 84.65423 | 1452.84 | 52.65988 | 1452.84 | 56.0462 | 1452.84 | -71.5832 |  | 1452.84 | 35.33085 |
| 1452.89 | -1.63588 | 1453.58 | -66.4324 | 1453.49 | 20.0024 | 1453.49 | 84.23456 | 1453.49 | 53.01226 | 1453.49 | 55.34231 | 1453.49 | -71.2193 |  | 1453.49 | 34.23698 |
| 1453.54 | -1.48974 | 1454.23 | -66.5484 | 1454.15 | 18.20624 | 1454.15 | 83.30352 | 1454.15 | 50.63604 | 1454.15 | 54.12268 | 1454.15 | -73.5839 |  | 1454.15 | 32.41947 |
| 1454.2 | -1.34528 | 1454.89 | -66.4929 | 1454.8 | 17.56838 | 1454.8 | 82.35248 | 1454.8 | 50.54703 | 1454.8 | 52.88742 | 1454.8 | -73.6614 |  | 1454.8 | 31.76057 |
| 1454.85 | -1.20311 | 1455.54 | -66.9604 | 1455.45 | 18.19402 | 1455.45 | 82.70124 | 1455.45 | 48.88731 | 1455.45 | 52.95196 | 1455.45 | -75.3096 |  | 1455.45 | 32.36518 |
| 1455.51 | -1.06355 | 1456.19 | -67.6019 | 1456.11 | 16.57174 | 1456.11 | 82.44834 | 1456.11 | 48.28288 | 1456.11 | 52.41047 | 1456.11 | -75.9024 |  | 1456.11 | 30.72154 |
| 1456.16 | -0.92691 | 1456.85 | -68.4418 | 1456.76 | 15.53578 | 1456.76 | 83.10833 | 1456.76 | 47.71675 | 1456.76 | 52.78624 | 1456.76 | -76.457 |  | 1456.76 | 29.66455 |
| 1456.82 | -0.7933 | 1457.5 | -68.1736 | 1457.41 | 14.92854 | 1457.41 | 82.22773 | 1457.41 | 47.51777 | 1457.41 | 51.62142 | 1457.41 | -76.6445 |  | 1457.41 | 29.03628 |
| 1457.47 | -0.66279 | 1458.15 | -67.4612 | 1458.07 | 13.2165 | 1458.07 | 81.71184 | 1458.07 | 48.00281 | 1458.07 | 50.81694 | 1458.07 | -76.1478 |  | 1458.07 | 27.30288 |
| 1458.12 | -0.5355 | 1458.8 | -68.4792 | 1458.72 | 12.46648 | 1458.72 | 80.40686 | 1458.72 | 48.2378 | 1458.72 | 49.22775 | 1458.72 | -75.9013 |  | 1458.72 | 26.53183 |
| 1458.78 | -0.41175 | 1459.46 | -69.2242 | 1459.37 | 11.62134 | 1459.37 | 79.31791 | 1459.37 | 47.90112 | 1459.37 | 47.85458 | 1459.37 | -76.2265 |  | 1459.37 | 25.66566 |
| 1459.43 | -0.29193 | 1460.11 | -69.7085 | 1460.03 | 10.26925 | 1460.03 | 78.26568 | 1460.03 | 47.54206 | 1460.03 | 46.51375 | 1460.03 | -76.5739 |  | 1460.03 | 24.29222 |
| 1460.08 | -0.17646 | 1460.76 | -70.4273 | 1460.68 | 10.2329 | 1460.68 | 76.34843 | 1460.68 | 44.18601 | 1460.68 | 44.31229 | 1460.68 | -79.9184 |  | 1460.68 | 24.23483 |
| 1460.74 | -0.06567 | 1461.42 | -69.9196 | 1461.33 | 9.77555 | 1461.33 | 75.18765 | 1461.33 | 42.54974 | 1461.33 | 42.86729 | 1461.33 | -81.5432 |  | 1461.33 | 23.75645 |
| 1461.39 | 0.04024 | 1462.07 | -69.8932 | 1461.98 | 8.76613 | 1461.98 | 75.34563 | 1461.98 | 41.00857 | 1461.98 | 42.74106 | 1461.98 | -83.0729 |  | 1461.98 | 22.72599 |
| 1462.04 | 0.14121 | 1462.72 | -69.3789 | 1462.64 | 8.33976 | 1462.64 | 75.44029 | 1462.64 | 40.11417 | 1462.64 | 42.54713 | 1462.64 | -83.9556 |  | 1462.64 | 22.27826 |
| 1462.7 | 0.23715 | 1463.37 | -69.3744 | 1463.29 | 6.94893 | 1463.29 | 75.02685 | 1463.29 | 39.22463 | 1463.29 | 41.84946 | 1463.29 | -84.8336 |  | 1463.29 | 20.8664 |
| 1463.35 | 0.32826 | 1464.03 | -68.888 | 1463.94 | 7.20513 | 1463.94 | 72.73786 | 1463.94 | 38.11654 | 1463.94 | 39.27625 | 1463.94 | -85.9302 |  | 1463.94 | 21.10158 |
| 1464 | 0.41429 | 1464.68 | -69.6586 | 1464.6 | 6.42106 | 1464.6 | 70.82892 | 1464.6 | 35.21216 | 1464.6 | 37.07873 | 1464.6 | -88.8229 |  | 1464.6 | 20.29615 |
| 1464.66 | 0.49497 | 1465.33 | -70.1212 | 1465.25 | 6.04115 | 1465.25 | 70.18693 | 1465.25 | 33.25648 | 1465.25 | 36.15252 | 1465.25 | -90.7671 |  | 1465.25 | 19.89521 |
| 1465.31 | 0.57049 | 1465.98 | -69.4024 | 1465.9 | 4.3577 | 1465.9 | 68.89238 | 1465.9 | 32.459 | 1465.9 | 34.57376 | 1465.9 | -91.5531 |  | 1465.9 | 18.19072 |
| 1465.96 | 0.64099 | 1466.63 | -68.7412 | 1466.55 | 3.6552 | 1466.55 | 67.15523 | 1466.55 | 31.18729 | 1466.55 | 32.55239 | 1466.55 | -92.8133 |  | 1466.55 | 17.46719 |
| 1466.62 | 0.7068 | 1467.29 | -68.6839 | 1467.21 | 4.93732 | 1467.21 | 66.1024 | 1467.21 | 29.41156 | 1467.21 | 31.21097 | 1467.21 | -94.5774 |  | 1467.21 | 18.72795 |
| 1467.27 | 0.76801 | 1467.94 | -68.8701 | 1467.86 | 4.28675 | 1467.86 | 64.56676 | 1467.86 | 28.73618 | 1467.86 | 29.39111 | 1467.86 | -95.2413 |  | 1467.86 | 18.05635 |
| 1467.92 | 0.82464 | 1468.59 | -69.3135 | 1468.51 | 3.8189 | 1468.51 | 63.07852 | 1468.51 | 28.52402 | 1468.51 | 27.61864 | 1468.51 | -95.4419 |  | 1468.51 | 17.56747 |
| 1468.58 | 0.87651 | 1469.24 | -69.3043 | 1469.16 | 3.50887 | 1469.16 | 62.48929 | 1469.16 | 28.38163 | 1469.16 | 26.7452 | 1469.16 | -95.5728 |  | 1469.16 | 17.23641 |
| 1469.23 | 0.92383 | 1469.89 | -69.5058 | 1469.81 | 2.73757 | 1469.81 | 61.2551 | 1469.81 | 27.11768 | 1469.81 | 25.22679 | 1469.81 | -96.8253 |  | 1469.81 | 16.44407 |
| 1469.88 | 0.96632 | 1470.55 | -68.8557 | 1470.47 | 1.61048 | 1470.47 | 59.14229 | 1470.47 | 26.76247 | 1470.47 | 22.82539 | 1470.47 | -97.1688 |  | 1470.47 | 15.29563 |
| 1470.53 | 1.00411 | 1471.2 | -68.9068 | 1471.12 | 0.66012 | 1471.12 | 58.41726 | 1471.12 | 27.14093 | 1471.12 | 21.81614 | 1471.12 | -96.7789 |  | 1471.12 | 14.32423 |
| 1471.19 | 1.03707 | 1471.85 | -68.7337 | 1471.77 | 1.12855 | 1471.77 | 57.94413 | 1471.77 | 27.63261 | 1471.77 | 21.0588 | 1471.77 | -96.2757 |  | 1471.77 | 14.77164 |
| 1471.84 | 1.06524 | 1472.5 | -69.6897 | 1472.42 | 1.58657 | 1472.42 | 56.98076 | 1472.42 | 28.15418 | 1472.42 | 19.81121 | 1472.42 | -95.7426 |  | 1472.42 | 15.20862 |
| 1472.49 | 1.08879 | 1473.15 | -70.5703 | 1473.07 | 0.50223 | 1473.07 | 56.59189 | 1473.07 | 27.24434 | 1473.07 | 19.13812 | 1473.07 | -96.641 |  | 1473.07 | 14.10324 |
| 1473.14 | 1.10744 | 1473.8 | -69.8871 | 1473.73 | -0.04316 | 1473.73 | 56.634 | 1473.73 | 26.99422 | 1473.73 | 18.89164 | 1473.73 | -96.8794 |  | 1473.73 | 13.39843 |
| 1473.8 | 1.12196 | 1474.45 | -70.2603 | 1474.38 | 0.66427 | 1474.38 | 56.65933 | 1474.38 | 25.18141 | 1474.38 | 18.63276 | 1474.38 | -98.6807 |  | 1474.38 | 13.57202 |
| 1474.45 | 1.13238 | 1475.1 | -69.3299 | 1475.03 | 1.16699 | 1475.03 | 55.90858 | 1475.03 | 24.48045 | 1475.03 | 17.59779 | 1475.03 | -99.3702 |  | 1475.03 | 13.54089 |
| 1475.1 | 1.13894 | 1475.76 | -69.8755 | 1475.68 | 2.70301 | 1475.68 | 55.54268 | 1475.68 | 25.65713 | 1475.68 | 16.94767 | 1475.68 | -98.182 |  | 1475.68 | 14.54307 |
| 1475.75 | 1.14171 | 1476.41 | -69.6984 | 1476.33 | 2.8941 | 1476.33 | 55.96358 | 1476.33 | 24.85794 | 1476.33 | 17.08435 | 1476.33 | -98.9697 |  | 1476.33 | 14.20033 |
| 1476.41 | 1.14059 | 1477.06 | -69.5204 | 1476.98 | 3.68891 | 1476.98 | 55.12468 | 1476.98 | 25.07528 | 1476.98 | 15.96123 | 1476.98 | -98.7409 |  | 1476.98 | 14.4613 |
| 1477.06 | 1.13589 | 1477.71 | -69.9183 | 1477.63 | 4.85213 | 1477.63 | 55.21062 | 1477.63 | 26.87792 | 1477.63 | 15.76296 | 1477.63 | -96.9268 |  | 1477.63 | 15.09067 |
| 1477.71 | 1.12761 | 1478.36 | -69.4316 | 1478.29 | 5.30667 | 1478.29 | 55.14637 | 1478.29 | 29.03784 | 1478.29 | 15.41012 | 1478.29 | -94.7552 |  | 1478.29 | 15.00316 |
| 1478.36 | 1.11624 | 1479.01 | -68.8953 | 1478.94 | 6.5463 | 1478.94 | 54.15063 | 1478.94 | 28.85087 | 1478.94 | 14.13016 | 1478.94 | -94.9306 |  | 1478.94 | 15.70896 |
| 1479.01 | 1.10223 | 1479.66 | -69.0448 | 1479.59 | 8.61495 | 1479.59 | 53.09332 | 1479.59 | 27.54908 | 1479.59 | 12.78863 | 1479.59 | -96.2209 |  | 1479.59 | 17.24376 |
| 1479.66 | 1.08571 | 1480.31 | -69.7076 | 1480.24 | 10.69934 | 1480.24 | 51.99478 | 1480.24 | 25.37951 | 1480.24 | 11.40587 | 1480.24 | -98.379 |  | 1480.24 | 18.79431 |
| 1480.32 | 1.06719 | 1480.96 | -70.7865 | 1480.89 | 11.28157 | 1480.89 | 51.62795 | 1480.89 | 26.56877 | 1480.89 | 10.75482 | 1480.89 | -97.1783 |  | 1480.89 | 18.8427 |
| 1480.97 | 1.04682 | 1481.61 | -70.8464 | 1481.54 | 12.2684 | 1481.54 | 51.31876 | 1481.54 | 28.26556 | 1481.54 | 10.16142 | 1481.54 | -95.47 |  | 1481.54 | 19.29569 |
| 1481.62 | 1.0249 | 1482.26 | -70.7102 | 1482.19 | 13.07189 | 1482.19 | 51.97834 | 1482.19 | 30.31431 | 1482.19 | 10.53678 | 1482.19 | -93.4097 |  | 1482.19 | 19.56534 |
| 1482.27 | 1.00192 | 1482.91 | -69.9159 | 1482.84 | 13.3148 | 1482.84 | 52.30041 | 1482.84 | 30.75796 | 1482.84 | 10.57463 | 1482.84 | -92.9546 |  | 1482.84 | 19.27441 |
| 1482.92 | 0.9783 | 1483.57 | -70.3663 | 1483.49 | 13.2981 | 1483.49 | 50.69204 | 1483.49 | 30.27533 | 1483.49 | 8.68204 | 1483.49 | -93.4257 |  | 1483.49 | 18.72387 |
| 1483.57 | 0.95427 | 1484.22 | -71.461 | 1484.14 | 13.72442 | 1484.14 | 50.05915 | 1484.14 | 30.02651 | 1484.14 | 7.76493 | 1484.14 | -93.6631 |  | 1484.14 | 18.61635 |
| 1484.23 | 0.93011 | 1484.87 | -71.4125 | 1484.79 | 14.88173 | 1484.79 | 47.95778 | 1484.79 | 30.11945 | 1484.79 | 5.37934 | 1484.79 | -93.5586 |  | 1484.79 | 19.23981 |
| 1484.88 | 0.90612 | 1485.52 | -71.3772 | 1485.44 | 15.91413 | 1485.44 | 47.98831 | 1485.44 | 30.17297 | 1485.44 | 5.12565 | 1485.44 | -93.4936 |  | 1485.44 | 19.73838 |
| 1485.53 | 0.88241 | 1486.17 | -72.0096 | 1486.1 | 16.96082 | 1486.1 | 47.35806 | 1486.1 | 30.25515 | 1486.1 | 4.20681 | 1486.1 | -93.3997 |  | 1486.1 | 20.24302 |
| 1486.18 | 0.85902 | 1486.82 | -70.7976 | 1486.75 | 17.68479 | 1486.75 | 47.11475 | 1486.75 | 29.6677 | 1486.75 | 3.67929 | 1486.75 | -93.9757 |  | 1486.75 | 20.43315 |
| 1486.83 | 0.83638 | 1487.47 | -68.939 | 1487.4 | 18.86414 | 1487.4 | 46.56046 | 1487.4 | 30.29052 | 1487.4 | 2.84078 | 1487.4 | -93.3414 |  | 1487.4 | 21.07866 |
| 1487.48 | 0.81463 | 1488.12 | -68.127 | 1488.05 | 17.87201 | 1488.05 | 46.99827 | 1488.05 | 29.81674 | 1488.05 | 2.99438 | 1488.05 | -93.8037 |  | 1488.05 | 19.55268 |
| 1488.13 | 0.7939 | 1488.77 | -67.7247 | 1488.7 | 17.70321 | 1488.7 | 46.51622 | 1488.7 | 29.50003 | 1488.7 | 2.22811 | 1488.7 | -94.1089 |  | 1488.7 | 18.85004 |
| 1488.78 | 0.77446 | 1489.42 | -68.0234 | 1489.35 | 17.79989 | 1489.35 | 46.50746 | 1489.35 | 27.78351 | 1489.35 | 1.93513 | 1489.35 | -95.8139 |  | 1489.35 | 18.41289 |
| 1489.43 | 0.75652 | 1490.07 | -68.1802 | 1490 | 17.45207 | 1490 | 45.35393 | 1490 | 27.42699 | 1490 | 0.49738 | 1490 | -96.1589 |  | 1490 | 17.53123 |
| 1490.08 | 0.74025 | 1490.72 | -67.7727 | 1490.65 | 17.17473 | 1490.65 | 45.2698 | 1490.65 | 28.46741 | 1490.65 | 0.12904 | 1490.65 | -95.107 |  | 1490.65 | 16.72004 |
| 1490.73 | 0.72574 | 1491.37 | -66.8076 | 1491.3 | 17.78366 | 1491.3 | 44.88235 | 1491.3 | 28.76175 | 1491.3 | -0.54264 | 1491.3 | -94.8012 |  | 1491.3 | 16.79513 |
| 1491.39 | 0.71331 | 1492.02 | -66.8106 | 1491.95 | 17.97934 | 1491.95 | 43.85018 | 1491.95 | 27.24303 | 1491.95 | -1.85902 | 1491.95 | -96.3084 |  | 1491.95 | 16.45697 |
| 1492.04 | 0.70353 | 1492.66 | -66.8838 | 1492.6 | 17.76855 | 1492.6 | 43.38665 | 1492.6 | 25.85705 | 1492.6 | -2.60677 | 1492.6 | -97.6829 |  | 1492.6 | 15.71234 |
| 1492.69 | 0.69665 | 1493.31 | -66.2182 | 1493.25 | 17.38815 | 1493.25 | 43.19723 | 1493.25 | 25.00696 | 1493.25 | -3.08041 | 1493.25 | -98.5215 |  | 1493.25 | 14.7981 |
| 1493.34 | 0.69273 | 1493.96 | -66.6766 | 1493.9 | 16.3805 | 1493.9 | 43.07585 | 1493.9 | 24.65706 | 1493.9 | -3.486 | 1493.9 | -98.8599 |  | 1493.9 | 13.25661 |
| 1493.99 | 0.69149 | 1494.61 | -67.4605 | 1494.55 | 16.65108 | 1494.55 | 42.00349 | 1494.55 | 23.75207 | 1494.55 | -4.84258 | 1494.55 | -99.7534 |  | 1494.55 | 12.99335 |
| 1494.64 | 0.69281 | 1495.26 | -68.009 | 1495.2 | 16.53705 | 1495.2 | 40.3031 | 1495.2 | 22.44675 | 1495.2 | -6.8272 | 1495.2 | -101.047 |  | 1495.2 | 12.34548 |
| 1495.29 | 0.6965 | 1495.91 | -68.5344 | 1495.85 | 16.30388 | 1495.85 | 38.10191 | 1495.85 | 20.20681 | 1495.85 | -9.3126 | 1495.85 | -103.276 |  | 1495.85 | 11.57847 |
| 1495.94 | 0.70267 | 1496.56 | -68.5187 | 1496.49 | 16.68347 | 1496.49 | 38.01871 | 1496.49 | 19.62743 | 1496.49 | -9.67564 | 1496.49 | -103.844 |  | 1496.49 | 11.43244 |
| 1496.59 | 0.71141 | 1497.21 | -68.9026 | 1497.14 | 16.52305 | 1497.14 | 36.77635 | 1497.14 | 19.26572 | 1497.14 | -11.2022 | 1497.14 | -104.194 |  | 1497.14 | 10.73817 |
| 1497.24 | 0.72292 | 1497.86 | -68.5606 | 1497.79 | 15.79772 | 1497.79 | 36.01576 | 1497.79 | 19.79186 | 1497.79 | -12.247 | 1497.79 | -103.656 |  | 1497.79 | 9.47901 |
| 1497.89 | 0.73686 | 1498.51 | -70.1315 | 1498.44 | 15.24268 | 1498.44 | 34.49379 | 1498.44 | 18.03807 | 1498.44 | -14.0532 | 1498.44 | -105.399 |  | 1498.44 | 8.39012 |
| 1498.54 | 0.75293 | 1499.16 | -70.3594 | 1499.09 | 15.8645 | 1499.09 | 33.49731 | 1499.09 | 16.43447 | 1499.09 | -15.3339 | 1499.09 | -106.991 |  | 1499.09 | 8.4781 |
| 1499.19 | 0.77115 | 1499.8 | -70.0291 | 1499.74 | 15.60357 | 1499.74 | 33.01397 | 1499.74 | 16.55794 | 1499.74 | -16.1015 | 1499.74 | -106.856 |  | 1499.74 | 7.68333 |
| 1499.84 | 0.7914 | 1500.45 | -69.9224 | 1500.39 | 14.47813 | 1500.39 | 31.82279 | 1500.39 | 16.47983 | 1500.39 | -17.5769 | 1500.39 | -106.922 |  | 1500.39 | 6.02405 |
| 1500.49 | 0.81422 | 1501.1 | -69.8456 | 1501.04 | 13.98964 | 1501.04 | 31.97004 | 1501.04 | 14.1316 | 1501.04 | -17.7138 | 1501.04 | -109.259 |  | 1501.04 | 5.00172 |
| 1501.14 | 0.83968 | 1501.75 | -70.78 | 1501.69 | 13.46134 | 1501.69 | 31.57885 | 1501.69 | 12.19004 | 1501.69 | -18.3892 | 1501.69 | -111.189 |  | 1501.69 | 3.93958 |
| 1501.79 | 0.86796 | 1502.4 | -70.8928 | 1502.34 | 12.09403 | 1502.34 | 30.66767 | 1502.34 | 11.11515 | 1502.34 | -19.5847 | 1502.34 | -112.253 |  | 1502.34 | 2.03843 |
| 1502.44 | 0.89901 | 1503.05 | -70.2314 | 1502.99 | 11.25053 | 1502.99 | 28.87099 | 1502.99 | 11.35229 | 1502.99 | -21.6655 | 1502.99 | -112.004 |  | 1502.99 | 0.66108 |
| 1503.08 | 0.93273 | 1503.7 | -71.0849 | 1503.64 | 11.62985 | 1503.64 | 26.97236 | 1503.64 | 9.93441 | 1503.64 | -23.8484 | 1503.64 | -113.41 |  | 1503.64 | 0.50657 |
| 1503.74 | 0.96911 | 1504.34 | -71.1819 | 1504.28 | 11.59449 | 1504.28 | 25.63308 | 1504.28 | 7.58553 | 1504.28 | -25.4675 | 1504.28 | -115.748 |  | 1504.28 | -0.05442 |
| 1504.38 | 1.00815 | 1504.99 | -72.6049 | 1504.93 | 10.22441 | 1504.93 | 23.54934 | 1504.93 | 6.27314 | 1504.93 | -27.8355 | 1504.93 | -117.049 |  | 1504.93 | -1.95834 |
| 1505.03 | 1.04978 | 1505.64 | -71.9446 | 1505.58 | 9.50334 | 1505.58 | 22.5611 | 1505.58 | 6.14703 | 1505.58 | -29.1079 | 1505.58 | -117.163 |  | 1505.58 | -3.21325 |
| 1505.68 | 1.094 | 1506.29 | -71.6453 | 1506.23 | 9.92804 | 1506.23 | 21.83658 | 1506.23 | 6.00432 | 1506.23 | -30.1167 | 1506.23 | -117.295 |  | 1506.23 | -3.32239 |
| 1506.33 | 1.14038 | 1506.94 | -72.7745 | 1506.88 | 9.77981 | 1506.88 | 20.35442 | 1506.88 | 5.15142 | 1506.88 | -31.8831 | 1506.88 | -118.136 |  | 1506.88 | -4.00447 |
| 1506.98 | 1.18862 | 1507.59 | -73.7893 | 1507.53 | 8.76804 | 1507.53 | 19.31578 | 1507.53 | 3.83695 | 1507.53 | -33.2059 | 1507.53 | -119.439 |  | 1507.53 | -5.55007 |
| 1507.63 | 1.23858 | 1508.23 | -74.5193 | 1508.17 | 7.51422 | 1508.17 | 17.05003 | 1508.17 | 3.74214 | 1508.17 | -35.7515 | 1508.17 | -119.522 |  | 1508.17 | -7.32952 |
| 1508.28 | 1.29024 | 1508.88 | -73.6836 | 1508.82 | 6.72352 | 1508.82 | 15.41198 | 1508.82 | 1.94637 | 1508.82 | -37.6738 | 1508.82 | -121.307 |  | 1508.82 | -8.65406 |
| 1508.93 | 1.34334 | 1509.53 | -73.9472 | 1509.47 | 6.31419 | 1509.47 | 13.48021 | 1509.47 | 1.61079 | 1509.47 | -39.8898 | 1509.47 | -121.631 |  | 1509.47 | -9.59723 |
| 1509.58 | 1.39772 | 1510.18 | -74.5091 | 1510.12 | 6.00083 | 1510.12 | 13.1 | 1510.12 | 0 | 1510.12 | -40.5542 | 1510.12 | -123.23 |  | 1510.12 | -10.4444 |
| 1510.22 | 1.45301 | 1510.82 | -74.5495 | 1510.77 | 5.30982 | 1510.77 | 10.44274 | 1510.77 | -1.42176 | 1510.77 | -43.4957 | 1510.77 | -126.313 |  | 1510.77 | -11.6693 |
| 1510.87 | 1.50906 | 1511.47 | -74.0145 | 1511.42 | 4.27693 | 1511.42 | 8.11704 | 1511.42 | -2.76246 | 1511.42 | -46.1056 | 1511.42 | -129.314 |  | 1511.42 | -13.236 |
| 1511.52 | 1.56551 | 1512.12 | -72.4001 | 1512.06 | 3.76427 | 1512.06 | 6.24227 | 1512.06 | -1.80107 | 1512.06 | -48.2602 | 1512.06 | -129.988 |  | 1512.06 | -14.2743 |
| 1512.17 | 1.62222 | 1512.77 | -72.7005 | 1512.71 | 2.28138 | 1512.71 | 5.61285 | 1512.71 | -0.31394 | 1512.71 | -49.1738 | 1512.71 | -130.162 |  | 1512.71 | -16.291 |
| 1512.82 | 1.67899 | 1513.41 | -73.5454 | 1513.36 | 1.1281 | 1513.36 | 5.50461 | 1513.36 | 0.96987 | 1513.36 | -49.5663 | 1513.36 | -130.539 |  | 1513.36 | -17.9782 |
| 1513.47 | 1.73534 | 1514.06 | -74.3989 | 1514.01 | 0.53306 | 1514.01 | 4.08048 | 1514.01 | 0.10054 | 1514.01 | -51.2746 | 1514.01 | -133.069 |  | 1514.01 | -19.107 |
| 1514.12 | 1.79081 | 1514.71 | -74.8903 | 1514.65 | 0 | 1514.65 | 2.25257 | 1514.65 | -1.1616 | 1514.65 | -53.3824 | 1514.65 | -135.967 |  | 1514.65 | -20.1657 |
| 1514.76 | 1.84559 | 1515.36 | -74.394 | 1515.3 | -0.29268 | 1515.3 | 0.94511 | 1515.3 | -2.44909 | 1515.3 | -54.9741 | 1515.3 | -138.915 |  | 1515.3 | -21.5224 |
| 1515.41 | 1.89947 | 1516 | -74.9197 | 1515.95 | -0.79086 | 1515.95 | 0 | 1515.95 | -2.88698 | 1515.95 | -56.2034 | 1515.95 | -141.014 |  | 1515.95 | -23.0845 |
| 1516.06 | 1.95235 | 1516.65 | -74.9546 | 1516.6 | -0.4764 | 1516.6 | 0.91552 | 1516.6 | -2.20557 | 1516.6 | -56.8257 | 1516.6 | -141.993 |  | 1516.6 | -23.834 |
| 1516.71 | 2.00459 | 1517.3 | -75.4067 | 1517.24 | -0.83184 | 1517.24 | 0.70404 | 1517.24 | -2.09854 | 1517.24 | -58.5513 | 1517.24 | -143.522 |  | 1517.24 | -25.237 |
| 1517.36 | 2.05599 | 1517.95 | -74.8216 | 1517.89 | -1.21032 | 1517.89 | 1.97818 | 1517.89 | -1.28694 | 1517.89 | -58.8149 | 1517.89 | -144.371 |  | 1517.89 | -26.6795 |
| 1518.01 | 2.1065 | 1518.59 | -75.128 | 1518.54 | -1.09029 | 1518.54 | 1.76703 | 1518.54 | 0.16827 | 1518.54 | -60.5638 | 1518.54 | -144.577 |  | 1518.54 | -27.6234 |
| 1518.65 | 2.1561 | 1519.24 | -76.8452 | 1519.19 | -0.83732 | 1519.19 | 1.74235 | 1519.19 | 1.05033 | 1519.19 | -62.1263 | 1519.19 | -145.355 |  | 1519.19 | -28.4344 |
| 1519.3 | 2.20633 | 1519.89 | -76.4981 | 1519.83 | -0.98886 | 1519.83 | 1.43205 | 1519.83 | 1.14202 | 1519.83 | -63.9507 | 1519.83 | -146.899 |  | 1519.83 | -29.6335 |
| 1519.95 | 2.25702 | 1520.53 | -76.16 | 1520.48 | -0.57168 | 1520.48 | 1.52011 | 1520.48 | 1.06593 | 1520.48 | -65.4004 | 1520.48 | -148.636 |  | 1520.48 | -30.2803 |
| 1520.6 | 2.30827 | 1521.18 | -74.8756 | 1521.13 | 1.35588 | 1521.13 | 0.94073 | 1521.13 | 0.31965 | 1521.13 | -67.5176 | 1521.13 | -151.043 |  | 1521.13 | -29.4167 |
| 1521.24 | 2.35997 | 1521.83 | -74.688 | 1521.78 | 2.28385 | 1521.78 | -0.01474 | 1521.78 | -0.7135 | 1521.78 | -70.0109 | 1521.78 | -153.737 |  | 1521.78 | -29.5527 |
| 1521.89 | 2.41157 | 1522.47 | -75.1917 | 1522.42 | 2.30827 | 1522.42 | -0.69465 | 1522.42 | 0.23963 | 1522.42 | -72.2049 | 1522.42 | -154.419 |  | 1522.42 | -30.5758 |
| 1522.54 | 2.4634 | 1523.12 | -75.0355 | 1523.07 | 3.2969 | 1523.07 | -0.81913 | 1523.07 | 0.91754 | 1523.07 | -73.8672 | 1523.07 | -155.402 |  | 1523.07 | -30.6512 |
| 1523.19 | 2.51538 | 1523.77 | -74.4502 | 1523.72 | 3.57102 | 1523.72 | -2.19107 | 1523.72 | -0.15377 | 1523.72 | -76.7769 | 1523.72 | -158.134 |  | 1523.72 | -31.441 |
| 1523.84 | 2.56758 | 1524.41 | -75.1763 | 1524.36 | 3.11279 | 1524.36 | -2.5298 | 1524.36 | 0.30767 | 1524.36 | -78.6297 | 1524.36 | -159.308 |  | 1524.36 | -32.9468 |
| 1524.48 | 2.61979 | 1525.06 | -75.7448 | 1525.01 | 4.17632 | 1525.01 | -2.38684 | 1525.01 | -0.05246 | 1525.01 | -80.0246 | 1525.01 | -161.329 |  | 1525.01 | -32.9472 |
| 1525.13 | 2.67218 | 1525.71 | -75.6174 | 1525.66 | 4.07778 | 1525.66 | -3.87603 | 1525.66 | -0.2437 | 1525.66 | -83.0515 | 1525.66 | -163.181 |  | 1525.66 | -34.1097 |
| 1525.78 | 2.72506 | 1526.35 | -75.8058 | 1526.3 | 4.99327 | 1526.3 | -4.21986 | 1526.3 | 0.21873 | 1526.3 | -84.9095 | 1526.3 | -164.354 |  | 1526.3 | -34.2418 |
| 1526.42 | 2.77873 | 1527 | -76.594 | 1526.95 | 5.2258 | 1526.95 | -4.03925 | 1526.95 | 0.63365 | 1526.95 | -86.2667 | 1526.95 | -165.6 |  | 1526.95 | -35.0733 |
| 1527.07 | 2.83305 | 1527.64 | -77.1312 | 1527.59 | 4.08333 | 1527.59 | -5.07602 | 1527.59 | 1.74948 | 1527.59 | -88.8176 | 1527.59 | -166.12 |  | 1527.59 | -37.2633 |
| 1527.72 | 2.88781 | 1528.29 | -77.2718 | 1528.24 | 3.62712 | 1528.24 | -5.36972 | 1528.24 | 2.23173 | 1528.24 | -90.649 | 1528.24 | -167.298 |  | 1528.24 | -38.7835 |
| 1528.36 | 2.94305 | 1528.94 | -77.0376 | 1528.89 | 3.9271 | 1528.89 | -5.87558 | 1528.89 | 4.12116 | 1528.89 | -92.6927 | 1528.89 | -167.07 |  | 1528.89 | -39.5475 |
| 1529.01 | 2.9987 | 1529.58 | -76.8607 | 1529.53 | 4.71668 | 1529.53 | -7.21902 | 1529.53 | 4.39785 | 1529.53 | -95.5502 | 1529.53 | -168.428 |  | 1529.53 | -39.8055 |
| 1529.66 | 3.05451 | 1530.23 | -77.2023 | 1530.18 | 4.11094 | 1530.18 | -6.89958 | 1530.18 | 5.44743 | 1530.18 | -96.7686 | 1530.18 | -169.04 |  | 1530.18 | -41.4752 |
| 1530.31 | 3.11074 | 1530.87 | -78.6296 | 1530.83 | 4.69285 | 1530.83 | -7.69897 | 1530.83 | 5.33407 | 1530.83 | -99.1058 | 1530.83 | -170.814 |  | 1530.83 | -41.9572 |
| 1530.95 | 3.16723 | 1531.52 | -78.4399 | 1531.47 | 4.1033 | 1531.47 | -8.4728 | 1531.47 | 5.32182 | 1531.47 | -101.394 | 1531.47 | -172.462 |  | 1531.47 | -43.5944 |
| 1531.6 | 3.22368 | 1532.16 | -79.4338 | 1532.12 | 3.45031 | 1532.12 | -9.68905 | 1532.12 | 4.19532 | 1532.12 | -104.148 | 1532.12 | -175.249 |  | 1532.12 | -45.3113 |
| 1532.25 | 3.27988 | 1532.81 | -79.9688 | 1532.76 | 2.87927 | 1532.76 | -9.10681 | 1532.76 | 1.83059 | 1532.76 | -105.08 | 1532.76 | -179.249 |  | 1532.76 | -46.9299 |
| 1532.89 | 3.33594 | 1533.46 | -80.6157 | 1533.41 | 1.92402 | 1533.41 | -9.51384 | 1533.41 | 0.47573 | 1533.41 | -107.024 | 1533.41 | -182.265 |  | 1533.41 | -48.9491 |
| 1533.54 | 3.39189 | 1534.1 | -80.7819 | 1534.06 | 1.24287 | 1534.06 | -9.86578 | 1534.06 | 1.7246 | 1534.06 | -108.914 | 1534.06 | -182.677 |  | 1534.06 | -50.6942 |
| 1534.18 | 3.44829 | 1534.75 | -80.725 | 1534.7 | 0.90968 | 1534.7 | -9.35059 | 1534.7 | 1.9285 | 1534.7 | -109.913 | 1534.7 | -184.108 |  | 1534.7 | -52.075 |
| 1534.83 | 3.50523 | 1535.39 | -80.1297 | 1535.35 | 1.38902 | 1535.35 | -9.11469 | 1535.35 | 2.06254 | 1535.35 | -111.215 | 1535.35 | -185.635 |  | 1535.35 | -52.6596 |
| 1535.48 | 3.56298 | 1536.04 | -81.3432 | 1535.99 | 2.1856 | 1535.99 | -8.76381 | 1535.99 | 2.08503 | 1535.99 | -112.378 | 1535.99 | -187.248 |  | 1535.99 | -52.9107 |
| 1536.12 | 3.6213 | 1536.68 | -82.1788 | 1536.64 | 2.20827 | 1536.64 | -8.98301 | 1536.64 | 2.20025 | 1536.64 | -114.135 | 1536.64 | -188.793 |  | 1536.64 | -53.9519 |
| 1536.77 | 3.68006 | 1537.33 | -82.2973 | 1537.28 | 1.35897 | 1537.28 | -8.41743 | 1537.28 | 2.13704 | 1537.28 | -115.084 | 1537.28 | -190.492 |  | 1537.28 | -55.8488 |
| 1537.42 | 3.73915 | 1537.97 | -81.3557 | 1537.93 | 1.66867 | 1537.93 | -7.70996 | 1537.93 | 1.54908 | 1537.93 | -115.914 | 1537.93 | -192.741 |  | 1537.93 | -56.6031 |
| 1538.06 | 3.79856 | 1538.62 | -81.4976 | 1538.57 | 1.40592 | 1538.57 | -8.01104 | 1538.57 | 0.08517 | 1538.57 | -117.729 | 1538.57 | -195.84 |  | 1538.57 | -57.9134 |
| 1538.71 | 3.8582 | 1539.26 | -81.0169 | 1539.22 | 1.28739 | 1539.22 | -8.19475 | 1539.22 | -2.36653 | 1539.22 | -119.451 | 1539.22 | -199.953 |  | 1539.22 | -59.0959 |
| 1539.35 | 3.91791 | 1539.91 | -81.1116 | 1539.87 | 0.39199 | 1539.87 | -8.71531 | 1539.87 | -4.39626 | 1539.87 | -121.509 | 1539.87 | -203.643 |  | 1539.87 | -61.0553 |
| 1540 | 3.97739 | 1540.55 | -79.8321 | 1540.51 | -0.71047 | 1540.51 | -9.52307 | 1540.51 | -4.96362 | 1540.51 | -123.831 | 1540.51 | -205.846 |  | 1540.51 | -63.2053 |
| 1540.65 | 4.03667 | 1541.2 | -79.6642 | 1541.16 | -0.85657 | 1541.16 | -9.88167 | 1541.16 | -7.12093 | 1541.16 | -125.727 | 1541.16 | -209.664 |  | 1541.16 | -64.4154 |
| 1541.29 | 4.09577 | 1541.84 | -79.8408 | 1541.8 | -1.64433 | 1541.8 | -9.73982 | 1541.8 | -7.71574 | 1541.8 | -127.1 | 1541.8 | -211.894 |  | 1541.8 | -66.2507 |
| 1541.94 | 4.15503 | 1542.49 | -79.4757 | 1542.45 | -2.42701 | 1542.45 | -9.58627 | 1542.45 | -7.93003 | 1542.45 | -128.484 | 1542.45 | -213.769 |  | 1542.45 | -68.0974 |
| 1542.58 | 4.2139 | 1543.13 | -78.9192 | 1543.09 | -3.20507 | 1543.09 | -9.95598 | 1543.09 | -8.01477 | 1543.09 | -130.368 | 1543.09 | -215.489 |  | 1543.09 | -69.923 |
| 1543.23 | 4.27233 | 1543.78 | -78.1095 | 1543.74 | -4.11501 | 1543.74 | -9.96596 | 1543.74 | -7.59671 | 1543.74 | -131.915 | 1543.74 | -216.732 |  | 1543.74 | -71.8969 |
| 1543.87 | 4.33006 | 1544.42 | -77.5996 | 1544.38 | -4.93209 | 1544.38 | -9.01078 | 1544.38 | -7.43988 | 1544.38 | -132.474 | 1544.38 | -218.211 |  | 1544.38 | -73.7616 |
| 1544.52 | 4.38674 | 1545.06 | -79.3714 | 1545.03 | -6.35214 | 1545.03 | -8.69899 | 1545.03 | -7.34959 | 1545.03 | -133.7 | 1545.03 | -219.781 |  | 1545.03 | -76.2456 |
| 1545.16 | 4.44199 | 1545.71 | -79.3782 | 1545.67 | -7.31542 | 1545.67 | -9.25714 | 1545.67 | -6.76876 | 1545.67 | -135.773 | 1545.67 | -220.836 |  | 1545.67 | -78.2564 |
| 1545.81 | 4.49569 | 1546.35 | -79.2907 | 1546.31 | -7.43948 | 1546.31 | -9.98705 | 1546.31 | -6.88147 | 1546.31 | -138.017 | 1546.31 | -222.584 |  | 1546.31 | -79.4281 |
| 1546.46 | 4.54769 | 1547 | -79.8456 | 1546.96 | -8.60081 | 1546.96 | -9.21036 | 1546.96 | -5.82129 | 1546.96 | -138.778 | 1546.96 | -223.185 |  | 1546.96 | -81.6534 |
| 1547.1 | 4.59761 | 1547.64 | -80.9049 | 1547.6 | -9.18204 | 1547.6 | -8.90635 | 1547.6 | -5.73863 | 1547.6 | -139.988 | 1547.6 | -224.737 |  | 1547.6 | -83.2822 |
| 1547.75 | 4.64584 | 1548.29 | -81.3247 | 1548.25 | -9.73886 | 1548.25 | -8.53771 | 1548.25 | -6.20081 | 1548.25 | -141.157 | 1548.25 | -226.86 |  | 1548.25 | -84.903 |
| 1548.39 | 4.69231 | 1548.93 | -81.2294 | 1548.89 | -9.86374 | 1548.89 | -8.57487 | 1548.89 | -6.20768 | 1548.89 | -142.708 | 1548.89 | -228.502 |  | 1548.89 | -86.0754 |
| 1549.04 | 4.73678 | 1549.57 | -82.135 | 1549.54 | -9.44597 | 1549.54 | -8.49368 | 1549.54 | -7.18684 | 1549.54 | -144.165 | 1549.54 | -231.142 |  | 1549.54 | -86.7216 |
| 1549.68 | 4.77922 | 1550.22 | -82.24 | 1550.18 | -9.7579 | 1550.18 | -8.15281 | 1550.18 | -6.92881 | 1550.18 | -145.338 | 1550.18 | -232.52 |  | 1550.18 | -88.0812 |
| 1550.33 | 4.81979 | 1550.86 | -82.4861 | 1550.83 | -10.1173 | 1550.83 | -8.32573 | 1550.83 | -8.12084 | 1550.83 | -147.049 | 1550.83 | -235.373 |  | 1550.83 | -89.5045 |
| 1550.97 | 4.85817 | 1551.5 | -82.913 | 1551.47 | -8.82895 | 1551.47 | -8.2227 | 1551.47 | -8.36371 | 1551.47 | -148.46 | 1551.47 | -237.251 |  | 1551.47 | -89.2637 |
| 1551.62 | 4.89382 | 1552.15 | -82.1636 | 1552.11 | -8.48404 | 1552.11 | -7.99183 | 1552.11 | -8.35965 | 1552.11 | -149.743 | 1552.11 | -238.882 |  | 1552.11 | -89.9664 |
| 1552.26 | 4.92639 | 1552.79 | -83.2326 | 1552.76 | -7.67089 | 1552.76 | -9.31259 | 1552.76 | -7.5056 | 1552.76 | -152.602 | 1552.76 | -239.689 |  | 1552.76 | -90.2172 |
| 1552.9 | 4.95545 | 1553.44 | -81.966 | 1553.4 | -7.70599 | 1553.4 | -9.618 | 1553.4 | -5.10604 | 1553.4 | -154.421 | 1553.4 | -238.925 |  | 1553.4 | -91.2999 |
| 1553.55 | 4.98109 | 1554.08 | -81.1856 | 1554.04 | -8.23383 | 1554.04 | -9.28771 | 1554.04 | -2.2261 | 1554.04 | -155.605 | 1554.04 | -237.68 |  | 1554.04 | -92.8754 |
| 1554.19 | 5.00316 | 1554.72 | -81.2826 | 1554.69 | -7.84149 | 1554.69 | -8.35044 | 1554.69 | 0.17794 | 1554.69 | -156.206 | 1554.69 | -236.651 |  | 1554.69 | -93.547 |
| 1554.84 | 5.02151 | 1555.37 | -80.2299 | 1555.33 | -6.89482 | 1555.33 | -8.42074 | 1555.33 | 0.0637 | 1555.33 | -157.79 | 1555.33 | -236.77 |  | 1555.33 | -93.6479 |
| 1555.48 | 5.03581 | 1556.01 | -80.369 | 1555.98 | -5.95288 | 1555.98 | -7.65916 | 1555.98 | -1.42257 | 1555.98 | -158.566 | 1555.98 | -238.26 |  | 1555.98 | -93.7699 |
| 1556.13 | 5.04596 | 1556.65 | -82.2759 | 1556.62 | -4.51623 | 1556.62 | -5.7526 | 1556.62 | -0.90666 | 1556.62 | -158.174 | 1556.62 | -237.748 |  | 1556.62 | -93.3808 |
| 1556.77 | 5.05196 | 1557.3 | -82.9083 | 1557.26 | -3.91587 | 1557.26 | -4.59487 | 1557.26 | -1.00605 | 1557.26 | -158.53 | 1557.26 | -237.852 |  | 1557.26 | -93.8281 |
| 1557.42 | 5.05387 | 1557.94 | -83.2616 | 1557.91 | -4.11944 | 1557.91 | -2.37563 | 1557.91 | 1.09626 | 1557.91 | -157.849 | 1557.91 | -235.754 |  | 1557.91 | -95.0956 |
| 1558.06 | 5.05131 | 1558.58 | -83.9171 | 1558.55 | -3.72064 | 1558.55 | -0.60574 | 1558.55 | 2.59471 | 1558.55 | -157.593 | 1558.55 | -234.259 |  | 1558.55 | -95.7444 |
| 1558.7 | 5.04411 | 1559.23 | -84.7349 | 1559.19 | -3.53019 | 1559.19 | -0.01981 | 1559.19 | 3.2803 | 1559.19 | -158.493 | 1559.19 | -233.578 |  | 1559.19 | -96.6015 |
| 1559.35 | 5.03201 | 1559.87 | -82.7881 | 1559.84 | -2.75042 | 1559.84 | -0.15403 | 1559.84 | 5.52026 | 1559.84 | -158.012 | 1559.84 | -231.342 |  | 1559.84 | -96.8857 |
| 1559.99 | 5.01533 | 1560.51 | -84.914 | 1560.48 | 0.20331 | 1560.48 | 0.36435 | 1560.48 | 5.00181 | 1560.48 | -156.887 | 1560.48 | -231.864 |  | 1560.48 | -94.8408 |
| 1560.64 | 4.994 | 1561.15 | -85.0996 | 1561.12 | 0.96386 | 1561.12 | 0.35588 | 1561.12 | 7.02884 | 1561.12 | -156.289 | 1561.12 | -229.841 |  | 1561.12 | -93.8734 |
| 1561.28 | 4.96789 | 1561.8 | -84.4826 | 1561.77 | 0.65851 | 1561.77 | 0.37342 | 1561.77 | 9.64993 | 1561.77 | -155.656 | 1561.77 | -227.224 |  | 1561.77 | -93.9686 |
| 1561.92 | 4.93701 | 1562.44 | -84.3605 | 1562.41 | 0.64984 | 1562.41 | 0.43024 | 1562.41 | 11.84167 | 1562.41 | -154.992 | 1562.41 | -225.037 |  | 1562.41 | -93.7703 |
| 1562.57 | 4.90113 | 1563.08 | -83.7211 | 1563.05 | 0.93353 | 1563.05 | 0.59705 | 1563.05 | 14.374 | 1563.05 | -154.219 | 1563.05 | -222.509 |  | 1563.05 | -93.2797 |
| 1563.21 | 4.86016 | 1563.72 | -83.6244 | 1563.7 | 1.31504 | 1563.7 | 0.58675 | 1563.7 | 17.38431 | 1563.7 | -153.614 | 1563.7 | -219.502 |  | 1563.7 | -92.6881 |
| 1563.85 | 4.81424 | 1564.37 | -83.3641 | 1564.34 | 2.70371 | 1564.34 | 0.82278 | 1564.34 | 19.43809 | 1564.34 | -152.771 | 1564.34 | -217.453 |  | 1564.34 | -91.0925 |
| 1564.5 | 4.76311 | 1565.01 | -84.2463 | 1564.98 | 3.8407 | 1564.98 | 2.1645 | 1564.98 | 22.43958 | 1564.98 | -150.823 | 1564.98 | -214.455 |  | 1564.98 | -89.7486 |
| 1565.14 | 4.70647 | 1565.65 | -84.2576 | 1565.62 | 4.56985 | 1565.62 | 2.43191 | 1565.62 | 26.83049 | 1565.62 | -149.949 | 1565.62 | -210.068 |  | 1565.62 | -88.8125 |
| 1565.78 | 4.64382 | 1566.29 | -82.8891 | 1566.27 | 6.33134 | 1566.27 | 3.06004 | 1566.27 | 30.97605 | 1566.27 | -148.705 | 1566.27 | -205.927 |  | 1566.27 | -86.8409 |
| 1566.43 | 4.5752 | 1566.94 | -82.5437 | 1566.91 | 8.129 | 1566.91 | 2.23234 | 1566.91 | 35.01056 | 1566.91 | -148.927 | 1566.91 | -201.897 |  | 1566.91 | -84.8363 |
| 1567.07 | 4.50058 | 1567.58 | -81.8426 | 1567.55 | 9.17538 | 1567.55 | 0.74446 | 1567.55 | 37.08142 | 1567.55 | -149.808 | 1567.55 | -199.83 |  | 1567.55 | -83.583 |
| 1567.71 | 4.4204 | 1568.22 | -82.3705 | 1568.19 | 10.5303 | 1568.19 | 0.74461 | 1568.19 | 39.94809 | 1568.19 | -149.201 | 1568.19 | -196.967 |  | 1568.19 | -82.0212 |
| 1568.36 | 4.33462 | 1568.86 | -81.871 | 1568.84 | 11.14041 | 1568.84 | 1.30685 | 1568.84 | 42.33875 | 1568.84 | -148.023 | 1568.84 | -194.581 |  | 1568.84 | -81.2009 |
| 1569 | 4.2434 | 1569.5 | -83.2496 | 1569.48 | 12.26483 | 1569.48 | 1.62014 | 1569.48 | 45.64451 | 1569.48 | -147.104 | 1569.48 | -191.279 |  | 1569.48 | -79.8696 |
| 1569.64 | 4.14674 | 1570.15 | -84.5371 | 1570.12 | 13.66846 | 1570.12 | 0.84107 | 1570.12 | 47.95145 | 1570.12 | -147.276 | 1570.12 | -188.976 |  | 1570.12 | -78.2591 |
| 1570.29 | 4.04494 | 1570.79 | -84.121 | 1570.76 | 14.09542 | 1570.76 | 1.42475 | 1570.76 | 52.168 | 1570.76 | -146.086 | 1570.76 | -184.764 |  | 1570.76 | -77.6252 |
| 1570.93 | 3.93775 | 1571.43 | -83.7054 | 1571.41 | 14.48179 | 1571.41 | 0.95955 | 1571.41 | 56.90096 | 1571.41 | -145.936 | 1571.41 | -180.035 |  | 1571.41 | -77.0287 |
| 1571.57 | 3.82526 | 1572.07 | -82.9914 | 1572.05 | 15.07256 | 1572.05 | 1.50774 | 1572.05 | 61.39641 | 1572.05 | -144.781 | 1572.05 | -175.543 |  | 1572.05 | -76.231 |
| 1572.21 | 3.70767 | 1572.71 | -82.3674 | 1572.69 | 16.39812 | 1572.69 | 3.3071 | 1572.69 | 66.0986 | 1572.69 | -142.375 | 1572.69 | -170.845 |  | 1572.69 | -74.6985 |
| 1572.86 | 3.58491 | 1573.36 | -83.1354 | 1573.33 | 18.05114 | 1573.33 | 3.46333 | 1573.33 | 70.95157 | 1573.33 | -141.613 | 1573.33 | -165.996 |  | 1573.33 | -72.8386 |
| 1573.5 | 3.45728 | 1574 | -83.383 | 1573.97 | 19.53317 | 1573.97 | 5.32015 | 1573.97 | 74.52709 | 1573.97 | -139.149 | 1573.97 | -162.425 |  | 1573.97 | -71.1497 |
| 1574.14 | 3.32531 | 1574.64 | -84.3691 | 1574.62 | 19.44579 | 1574.62 | 6.4018 | 1574.62 | 79.43373 | 1574.62 | -137.452 | 1574.62 | -157.522 |  | 1574.62 | -71.0269 |
| 1574.79 | 3.18959 | 1575.28 | -85.9102 | 1575.26 | 20.95712 | 1575.26 | 7.18705 | 1575.26 | 83.30419 | 1575.26 | -136.06 | 1575.26 | -153.656 |  | 1575.26 | -69.3087 |
| 1575.43 | 3.05031 | 1575.92 | -86.1538 | 1575.9 | 22.66179 | 1575.9 | 8.50132 | 1575.9 | 88.46127 | 1575.9 | -134.14 | 1575.9 | -148.503 |  | 1575.9 | -67.3971 |
| 1576.07 | 2.90759 | 1576.56 | -85.8991 | 1576.54 | 24.73282 | 1576.54 | 9.70774 | 1576.54 | 90.44504 | 1576.54 | -132.327 | 1576.54 | -146.523 |  | 1576.54 | -65.1191 |
| 1576.71 | 2.76145 | 1577.2 | -85.7856 | 1577.18 | 26.13286 | 1577.18 | 9.39867 | 1577.18 | 94.73838 | 1577.18 | -132.029 | 1577.18 | -142.234 |  | 1577.18 | -63.5122 |
| 1577.35 | 2.61166 | 1577.84 | -86.2518 | 1577.82 | 28.58016 | 1577.82 | 10.58216 | 1577.82 | 98.21755 | 1577.82 | -130.24 | 1577.82 | -138.759 |  | 1577.82 | -60.858 |
| 1578 | 2.45817 | 1578.49 | -86.2038 | 1578.47 | 30.99334 | 1578.47 | 10.89636 | 1578.47 | 101.0615 | 1578.47 | -129.309 | 1578.47 | -135.919 |  | 1578.47 | -58.2347 |
| 1578.64 | 2.30081 | 1579.13 | -87.1102 | 1579.11 | 32.09464 | 1579.11 | 12.85415 | 1579.11 | 105.8978 | 1579.11 | -126.745 | 1579.11 | -131.087 |  | 1579.11 | -56.9264 |
| 1579.28 | 2.13978 | 1579.77 | -86.9174 | 1579.75 | 34.24045 | 1579.75 | 13.93921 | 1579.75 | 110.0675 | 1579.75 | -125.054 | 1579.75 | -126.921 |  | 1579.75 | -54.5737 |
| 1579.92 | 1.97527 | 1580.41 | -85.5865 | 1580.39 | 36.27673 | 1580.39 | 15.18857 | 1580.39 | 116.6184 | 1580.39 | -123.198 | 1580.39 | -120.374 |  | 1580.39 | -52.3305 |
| 1580.56 | 1.80747 | 1581.05 | -86.0224 | 1581.03 | 39.08438 | 1581.03 | 16.10911 | 1581.03 | 122.8447 | 1581.03 | -121.671 | 1581.03 | -114.152 |  | 1581.03 | -49.316 |
| 1581.21 | 1.63712 | 1581.69 | -86.6397 | 1581.67 | 41.76456 | 1581.67 | 18.01259 | 1581.67 | 128.2467 | 1581.67 | -119.161 | 1581.67 | -108.754 |  | 1581.67 | -46.4289 |
| 1581.85 | 1.46472 | 1582.33 | -85.4576 | 1582.31 | 44.47807 | 1582.31 | 19.85843 | 1582.31 | 135.3844 | 1582.31 | -116.709 | 1582.31 | -101.621 |  | 1582.31 | -43.5085 |
| 1582.49 | 1.29036 | 1582.97 | -87.245 | 1582.95 | 47.63578 | 1582.95 | 21.36132 | 1582.95 | 140.5356 | 1582.95 | -114.6 | 1582.95 | -96.4735 |  | 1582.95 | -40.1438 |
| 1583.13 | 1.11451 | 1583.61 | -87.5996 | 1583.59 | 50.06505 | 1583.59 | 23.28853 | 1583.59 | 147.5544 | 1583.59 | -112.066 | 1583.59 | -89.4587 |  | 1583.59 | -37.5077 |
| 1583.77 | 0.93763 | 1584.25 | -88.6795 | 1584.24 | 50.67558 | 1584.24 | 25.02018 | 1584.24 | 152.4079 | 1584.24 | -109.719 | 1584.24 | -84.6093 |  | 1584.24 | -36.687 |
| 1584.41 | 0.7601 | 1584.89 | -89.1633 | 1584.88 | 52.07386 | 1584.88 | 26.83386 | 1584.88 | 156.6484 | 1584.88 | -107.298 | 1584.88 | -80.3729 |  | 1584.88 | -35.0818 |
| 1585.06 | 0.5817 | 1585.53 | -88.5016 | 1585.52 | 54.12887 | 1585.52 | 29.4942 | 1585.52 | 160.6242 | 1585.52 | -104.032 | 1585.52 | -76.4012 |  | 1585.52 | -32.8199 |
| 1585.7 | 0.40246 | 1586.17 | -86.0863 | 1586.16 | 55.50055 | 1586.16 | 32.50965 | 1586.16 | 164.6035 | 1586.16 | -100.41 | 1586.16 | -72.426 |  | 1586.16 | -31.2413 |
| 1586.34 | 0.22245 | 1586.82 | -87.4937 | 1586.8 | 57.39516 | 1586.8 | 35.5347 | 1586.8 | 168.549 | 1586.8 | -96.7784 | 1586.8 | -68.4845 |  | 1586.8 | -29.1398 |
| 1586.98 | 0.042 | 1587.46 | -89.5733 | 1587.44 | 57.38261 | 1587.44 | 36.02112 | 1587.44 | 172.4556 | 1587.44 | -95.6856 | 1587.44 | -64.582 |  | 1587.44 | -28.9454 |
| 1587.62 | -0.13884 | 1588.1 | -89.6179 | 1588.08 | 58.16073 | 1588.08 | 39.59146 | 1588.08 | 175.6446 | 1588.08 | -91.5089 | 1588.08 | -61.397 |  | 1588.08 | -27.9604 |
| 1588.26 | -0.31992 | 1588.74 | -88.5906 | 1588.72 | 60.98904 | 1588.72 | 40.56925 | 1588.72 | 180.5214 | 1588.72 | -89.9247 | 1588.72 | -56.5243 |  | 1588.72 | -24.9252 |
| 1588.9 | -0.50105 | 1589.38 | -88.5152 | 1589.36 | 62.65205 | 1589.36 | 41.10489 | 1589.36 | 183.7427 | 1589.36 | -88.7827 | 1589.36 | -53.3071 |  | 1589.36 | -23.0552 |
| 1589.54 | -0.68237 | 1590.02 | -87.2698 | 1590 | 64.60034 | 1590 | 42.94484 | 1590 | 188.431 | 1590 | -86.3363 | 1590 | -48.6229 |  | 1590 | -20.9 |
| 1590.19 | -0.86371 | 1590.66 | -86.0141 | 1590.64 | 66.45373 | 1590.64 | 42.99499 | 1590.64 | 191.301 | 1590.64 | -85.6798 | 1590.64 | -45.757 |  | 1590.64 | -18.8397 |
| 1590.83 | -1.04464 | 1591.3 | -85.2423 | 1591.28 | 67.84346 | 1591.28 | 45.60396 | 1591.28 | 193.1606 | 1591.28 | -82.4644 | 1591.28 | -43.9014 |  | 1591.28 | -17.2431 |
| 1591.47 | -1.22502 | 1591.94 | -84.3436 | 1591.92 | 68.9128 | 1591.92 | 46.2319 | 1591.92 | 196.0376 | 1591.92 | -81.2301 | 1591.92 | -41.0284 |  | 1591.92 | -15.9668 |
| 1592.11 | -1.4048 | 1592.58 | -85.1446 | 1592.56 | 70.46448 | 1592.56 | 46.01841 | 1592.56 | 198.7752 | 1592.56 | -80.8372 | 1592.56 | -38.2949 |  | 1592.56 | -14.2082 |
| 1592.75 | -1.58418 | 1593.21 | -85.5548 | 1593.2 | 70.63999 | 1593.2 | 47.46607 | 1593.2 | 203.0812 | 1593.2 | -78.7831 | 1593.2 | -33.9931 |  | 1593.2 | -13.8258 |
| 1593.39 | -1.7632 | 1593.85 | -84.591 | 1593.84 | 71.76236 | 1593.84 | 47.72798 | 1593.84 | 205.2282 | 1593.84 | -77.9148 | 1593.84 | -31.8501 |  | 1593.84 | -12.4966 |
| 1594.03 | -1.94171 | 1594.49 | -84.4879 | 1594.48 | 72.5002 | 1594.48 | 48.29553 | 1594.48 | 207.8374 | 1594.48 | -76.7408 | 1594.48 | -29.245 |  | 1594.48 | -11.5518 |
| 1594.67 | -2.1193 | 1595.13 | -84.715 | 1595.12 | 73.04578 | 1595.12 | 49.15597 | 1595.12 | 208.9956 | 1595.12 | -75.274 | 1595.12 | -28.0908 |  | 1595.12 | -10.7993 |
| 1595.31 | -2.29601 | 1595.77 | -84.4104 | 1595.76 | 74.3384 | 1595.76 | 49.90479 | 1595.76 | 209.9266 | 1595.76 | -73.9188 | 1595.76 | -27.1639 |  | 1595.76 | -9.29977 |
| 1595.95 | -2.47212 | 1596.41 | -83.7417 | 1596.4 | 74.55493 | 1596.4 | 50.38708 | 1596.4 | 210.8694 | 1596.4 | -72.8301 | 1596.4 | -26.2252 |  | 1596.4 | -8.87633 |
| 1596.59 | -2.64783 | 1597.05 | -83.8563 | 1597.04 | 75.92589 | 1597.04 | 50.986 | 1597.04 | 213.6877 | 1597.04 | -71.6248 | 1597.04 | -23.411 |  | 1597.04 | -7.29846 |
| 1597.23 | -2.82307 | 1597.69 | -84.5509 | 1597.68 | 76.89683 | 1597.68 | 51.36802 | 1597.68 | 215.7529 | 1597.68 | -70.6364 | 1597.68 | -21.3498 |  | 1597.68 | -6.12061 |
| 1597.87 | -2.99763 | 1598.33 | -83.716 | 1598.32 | 76.80385 | 1598.32 | 50.43958 | 1598.32 | 216.5885 | 1598.32 | -70.9584 | 1598.32 | -20.5182 |  | 1598.32 | -6.00668 |
| 1598.51 | -3.1715 | 1598.97 | -83.5509 | 1598.96 | 76.58399 | 1598.96 | 51.24208 | 1598.96 | 216.8782 | 1598.96 | -69.5495 | 1598.96 | -20.2326 |  | 1598.96 | -6.01963 |
| 1599.15 | -3.34489 | 1599.61 | -83.7144 | 1599.6 | 77.07276 | 1599.6 | 51.66844 | 1599.6 | 215.9412 | 1599.6 | -68.5167 | 1599.6 | -21.1737 |  | 1599.6 | -5.32395 |
| 1599.79 | -3.51755 | 1600.25 | -83.1452 | 1600.24 | 77.27947 | 1600.24 | 53.54555 | 1600.24 | 219.2572 | 1600.24 | -66.0332 | 1600.24 | -17.8618 |  | 1600.24 | -4.91033 |
| 1600.43 | -3.68981 | 1600.89 | -82.3771 | 1600.88 | 76.31155 | 1600.88 | 53.04967 | 1600.88 | 219.5899 | 1600.88 | -65.9227 | 1600.88 | -17.5331 |  | 1600.88 | -5.67134 |
| 1601.07 | -3.86163 | 1601.52 | -81.0178 | 1601.52 | 76.46304 | 1601.52 | 54.07884 | 1601.52 | 220.2952 | 1601.52 | -64.2871 | 1601.52 | -16.8319 |  | 1601.52 | -5.31294 |
| 1601.71 | -4.03321 | 1602.16 | -80.2793 | 1602.16 | 76.39197 | 1602.16 | 54.1103 | 1602.16 | 220.3513 | 1602.16 | -63.6493 | 1602.16 | -16.7798 |  | 1602.16 | -5.1771 |
| 1602.35 | -4.20447 | 1602.8 | -80.2008 | 1602.8 | 76.3606 | 1602.8 | 53.909 | 1602.8 | 221.7264 | 1602.8 | -63.2442 | 1602.8 | -15.4088 |  | 1602.8 | -5.00155 |
| 1602.99 | -4.37555 | 1603.44 | -80.4208 | 1603.43 | 77.04482 | 1603.43 | 53.18966 | 1603.43 | 220.6991 | 1603.43 | -63.3666 | 1603.43 | -16.4402 |  | 1603.43 | -4.11366 |
| 1603.63 | -4.54644 | 1604.08 | -81.6768 | 1604.07 | 76.48227 | 1604.07 | 54.23001 | 1604.07 | 217.1821 | 1604.07 | -61.7199 | 1604.07 | -19.9612 |  | 1604.07 | -4.4693 |
| 1604.27 | -4.71919 | 1604.19 | -82.6838 | 1604.71 | 75.49343 | 1604.71 | 53.89168 | 1604.71 | 215.7516 | 1604.71 | -61.4518 | 1604.71 | -21.3958 |  | 1604.71 | -5.25122 |
| 1604.91 | -4.89368 | 1604.83 | -82.4381 | 1605.35 | 75.79901 | 1605.35 | 53.29685 | 1605.35 | 215.6373 | 1605.35 | -61.4402 | 1605.35 | -21.5142 |  | 1605.35 | -4.73873 |
| 1605.55 | -5.06952 | 1605.47 | -82.3158 | 1605.99 | 75.80106 | 1605.99 | 53.63608 | 1605.99 | 212.8843 | 1605.99 | -60.4946 | 1605.99 | -24.2713 |  | 1605.99 | -4.52978 |
| 1606.19 | -5.24685 | 1606.11 | -82.1292 | 1606.63 | 75.4976 | 1606.63 | 52.18565 | 1606.63 | 212.342 | 1606.63 | -61.3386 | 1606.63 | -24.8176 |  | 1606.63 | -4.62632 |
| 1606.83 | -5.42548 | 1606.75 | -81.9795 | 1607.27 | 76.16003 | 1607.27 | 50.58693 | 1607.27 | 209.4603 | 1607.27 | -62.3309 | 1607.27 | -27.7034 |  | 1607.27 | -3.75699 |
| 1607.47 | -5.60516 | 1607.39 | -83.0956 | 1607.91 | 75.77451 | 1607.91 | 49.22544 | 1607.91 | 206.3803 | 1607.91 | -63.086 | 1607.91 | -30.7875 |  | 1607.91 | -3.9356 |
| 1608.11 | -5.78548 | 1608.03 | -85.0822 | 1608.55 | 74.48251 | 1608.55 | 48.71018 | 1608.55 | 202.8252 | 1608.55 | -62.9949 | 1608.55 | -34.3466 |  | 1608.55 | -5.02068 |
| 1608.75 | -5.96641 | 1608.67 | -85.4493 | 1609.18 | 73.99178 | 1609.18 | 48.33786 | 1609.18 | 202.7561 | 1609.18 | -62.7703 | 1609.18 | -34.4197 |  | 1609.18 | -5.30773 |
| 1609.39 | -6.14794 | 1609.31 | -86.3356 | 1609.82 | 74.08126 | 1609.82 | 48.94192 | 1609.82 | 199.6196 | 1609.82 | -61.5598 | 1609.82 | -37.5603 |  | 1609.82 | -5.01135 |
| 1610.03 | -6.33031 | 1609.95 | -85.9956 | 1610.46 | 74.5219 | 1610.46 | 48.49357 | 1610.46 | 197.737 | 1610.46 | -61.4018 | 1610.46 | -39.4469 |  | 1610.46 | -4.3638 |
| 1610.66 | -6.51399 | 1610.59 | -85.0797 | 1611.1 | 74.5641 | 1611.1 | 49.89262 | 1611.1 | 195.8805 | 1611.1 | -59.3963 | 1611.1 | -41.3075 |  | 1611.1 | -4.11469 |
| 1611.3 | -6.69913 | 1611.23 | -82.2209 | 1611.74 | 73.64189 | 1611.74 | 48.67675 | 1611.74 | 192.7557 | 1611.74 | -60.0058 | 1611.74 | -44.4364 |  | 1611.74 | -4.82998 |
| 1611.94 | -6.88605 | 1611.87 | -83.4962 | 1612.38 | 72.49753 | 1612.38 | 46.95944 | 1612.38 | 187.2858 | 1612.38 | -61.1167 | 1612.38 | -49.9103 |  | 1612.38 | -5.76743 |
| 1612.58 | -7.07507 | 1612.51 | -84.0245 | 1613.01 | 70.62444 | 1613.01 | 44.82195 | 1613.01 | 182.9306 | 1613.01 | -62.6573 | 1613.01 | -54.2696 |  | 1613.01 | -7.43685 |
| 1613.22 | -7.26633 | 1613.15 | -84.5296 | 1613.65 | 68.89274 | 1613.65 | 43.20888 | 1613.65 | 179.7497 | 1613.65 | -63.664 | 1613.65 | -57.4546 |  | 1613.65 | -8.96164 |
| 1613.86 | -7.45974 | 1613.79 | -85.0917 | 1614.29 | 67.07123 | 1614.29 | 40.35223 | 1614.29 | 178.1317 | 1614.29 | -65.9142 | 1614.29 | -59.0766 |  | 1614.29 | -10.5762 |
| 1614.5 | -7.65524 | 1614.43 | -84.543 | 1614.93 | 64.67913 | 1614.93 | 38.59395 | 1614.93 | 174.5277 | 1614.93 | -67.0661 | 1614.93 | -62.6847 |  | 1614.93 | -12.7614 |
| 1615.14 | -7.85274 | 1615.07 | -82.8987 | 1615.57 | 61.79224 | 1615.57 | 38.08232 | 1615.57 | 170.305 | 1615.57 | -66.9713 | 1615.57 | -66.9115 |  | 1615.57 | -15.4414 |
| 1615.78 | -8.05241 | 1615.71 | -84.1321 | 1616.2 | 59.98035 | 1616.2 | 36.4803 | 1616.2 | 165.2636 | 1616.2 | -67.9764 | 1616.2 | -71.9569 |  | 1616.2 | -17.0496 |
| 1616.41 | -8.25428 | 1616.35 | -82.3496 | 1616.84 | 57.82533 | 1616.84 | 35.37407 | 1616.84 | 162.0638 | 1616.84 | -68.4763 | 1616.84 | -75.1608 |  | 1616.84 | -18.9977 |
| 1617.05 | -8.45826 | 1616.99 | -83.202 | 1617.48 | 56.33777 | 1617.48 | 33.6674 | 1617.48 | 158.6081 | 1617.48 | -69.5765 | 1617.48 | -78.6205 |  | 1617.48 | -20.2784 |
| 1617.69 | -8.66428 | 1617.62 | -83.6659 | 1618.12 | 53.23667 | 1618.12 | 32.77381 | 1618.12 | 154.8604 | 1618.12 | -69.8637 | 1618.12 | -82.3722 |  | 1618.12 | -23.1726 |
| 1618.33 | -8.87266 | 1618.26 | -86.1213 | 1618.75 | 50.70422 | 1618.75 | 29.68359 | 1618.75 | 149.5425 | 1618.75 | -72.357 | 1618.75 | -87.6942 |  | 1618.75 | -25.5013 |
| 1618.97 | -9.08339 | 1618.9 | -86.4151 | 1619.39 | 49.82794 | 1619.39 | 26.89482 | 1619.39 | 145.7242 | 1619.39 | -74.5394 | 1619.39 | -91.5166 |  | 1619.39 | -26.1707 |
| 1619.6 | -9.29645 | 1619.54 | -86.2055 | 1620.03 | 49.13233 | 1620.03 | 26.73854 | 1620.03 | 141.0402 | 1620.03 | -74.0893 | 1620.03 | -96.2045 |  | 1620.03 | -26.6594 |
| 1620.24 | -9.51176 | 1620.18 | -86.2164 | 1620.67 | 47.80233 | 1620.67 | 23.48577 | 1620.67 | 136.5051 | 1620.67 | -76.7357 | 1620.67 | -100.744 |  | 1620.67 | -27.7825 |
| 1620.88 | -9.72931 | 1620.82 | -87.4671 | 1621.3 | 43.96261 | 1621.3 | 22.71928 | 1621.3 | 132.7832 | 1621.3 | -76.9052 | 1621.3 | -104.47 |  | 1621.3 | -31.4185 |
| 1621.52 | -9.94922 | 1621.46 | -88.1936 | 1621.94 | 41.59586 | 1621.94 | 22.45075 | 1621.94 | 128.2545 | 1621.94 | -76.5674 | 1621.94 | -109.002 |  | 1621.94 | -33.5784 |
| 1622.16 | -10.1717 | 1622.1 | -89.623 | 1622.58 | 39.62047 | 1622.58 | 21.27765 | 1622.58 | 123.3407 | 1622.58 | -77.1341 | 1622.58 | -113.92 |  | 1622.58 | -35.3469 |
| 1622.79 | -10.397 | 1622.74 | -89.964 | 1623.22 | 37.82206 | 1623.22 | 20.77099 | 1623.22 | 119.0743 | 1623.22 | -77.0343 | 1623.22 | -118.191 |  | 1623.22 | -36.9384 |
| 1623.43 | -10.6254 | 1623.38 | -91.665 | 1623.85 | 37.94491 | 1623.85 | 16.92022 | 1623.85 | 117.0519 | 1623.85 | -80.2882 | 1623.85 | -120.217 |  | 1623.85 | -36.6118 |
| 1624.07 | -10.8566 | 1624.01 | -91.6619 | 1624.49 | 37.4867 | 1624.49 | 16.47763 | 1624.49 | 112.5546 | 1624.49 | -80.1244 | 1624.49 | -124.719 |  | 1624.49 | -36.8631 |
| 1624.71 | -11.0907 | 1624.65 | -91.3744 | 1625.13 | 36.858 | 1625.13 | 14.74055 | 1625.13 | 105.8607 | 1625.13 | -81.255 | 1625.13 | -131.417 |  | 1625.13 | -37.2849 |
| 1625.35 | -11.3273 | 1625.29 | -91.7196 | 1625.76 | 35.24399 | 1625.76 | 11.78841 | 1625.76 | 100.2009 | 1625.76 | -83.6103 | 1625.76 | -137.08 |  | 1625.76 | -38.6953 |
| 1625.98 | -11.5666 | 1625.93 | -91.8746 | 1626.4 | 34.3451 | 1626.4 | 10.54016 | 1626.4 | 95.37618 | 1626.4 | -84.2521 | 1626.4 | -141.909 |  | 1626.4 | -39.3872 |
| 1626.62 | -11.809 | 1626.57 | -93.0979 | 1627.04 | 34.33091 | 1627.04 | 9.32015 | 1627.04 | 88.79915 | 1627.04 | -84.8657 | 1627.04 | -148.49 |  | 1627.04 | -39.1945 |
| 1627.26 | -12.0545 | 1627.21 | -92.4236 | 1627.67 | 32.84536 | 1627.67 | 8.14944 | 1627.67 | 83.93319 | 1627.67 | -85.4395 | 1627.67 | -153.36 |  | 1627.67 | -40.4764 |
| 1627.89 | -12.3029 | 1627.84 | -93.1133 | 1628.31 | 30.66815 | 1628.31 | 5.48062 | 1628.31 | 77.64886 | 1628.31 | -87.5019 | 1628.31 | -159.649 |  | 1628.31 | -42.4467 |
| 1628.53 | -12.5544 | 1628.48 | -93.7516 | 1628.95 | 30.34771 | 1628.95 | 2.54066 | 1628.95 | 72.37135 | 1628.95 | -89.8355 | 1628.95 | -164.93 |  | 1628.95 | -42.5602 |
| 1629.17 | -12.809 | 1629.12 | -92.9985 | 1629.58 | 27.37451 | 1629.58 | 0.01074 | 1629.58 | 67.09284 | 1629.58 | -91.7685 | 1629.58 | -170.213 |  | 1629.58 | -45.3297 |
| 1629.81 | -13.0669 | 1629.76 | -91.6393 | 1630.22 | 25.02936 | 1630.22 | -2.17589 | 1630.22 | 63.22788 | 1630.22 | -93.3487 | 1630.22 | -174.082 |  | 1630.22 | -47.468 |
| 1630.44 | -13.3278 | 1630.4 | -91.8664 | 1630.86 | 24.80755 | 1630.86 | -2.59879 | 1630.86 | 58.34881 | 1630.86 | -93.1652 | 1630.86 | -178.965 |  | 1630.86 | -47.4829 |
| 1631.08 | -13.5915 | 1631.04 | -91.538 | 1631.49 | 23.67751 | 1631.49 | -5.08866 | 1631.49 | 53.51139 | 1631.49 | -95.0582 | 1631.49 | -183.806 |  | 1631.49 | -48.4092 |
| 1631.72 | -13.8572 | 1631.67 | -90.4809 | 1632.13 | 21.86503 | 1632.13 | -6.05761 | 1632.13 | 49.81777 | 1632.13 | -95.4207 | 1632.13 | -187.504 |  | 1632.13 | -50.0148 |
| 1632.35 | -14.1246 | 1632.31 | -90.8122 | 1632.76 | 20.12636 | 1632.76 | -7.94238 | 1632.76 | 45.53663 | 1632.76 | -96.7086 | 1632.76 | -191.789 |  | 1632.76 | -51.5498 |
| 1632.99 | -14.3936 | 1632.95 | -90.6282 | 1633.4 | 19.82829 | 1633.4 | -8.21405 | 1633.4 | 40.85394 | 1633.4 | -96.3738 | 1633.4 | -196.476 |  | 1633.4 | -51.641 |
| 1633.63 | -14.6638 | 1633.59 | -90.0876 | 1634.04 | 18.77199 | 1634.04 | -10.8806 | 1634.04 | 34.46949 | 1634.04 | -98.434 | 1634.04 | -202.864 |  | 1634.04 | -52.4903 |
| 1634.26 | -14.9352 | 1634.22 | -90.2059 | 1634.67 | 18.04198 | 1634.67 | -11.0485 | 1634.67 | 29.31239 | 1634.67 | -98.005 | 1634.67 | -208.025 |  | 1634.67 | -53.0167 |
| 1634.9 | -15.2074 | 1634.86 | -90.2916 | 1635.31 | 17.66607 | 1635.31 | -11.3668 | 1635.31 | 23.11911 | 1635.31 | -97.7169 | 1635.31 | -214.223 |  | 1635.31 | -53.1857 |
| 1635.54 | -15.48 | 1635.5 | -90.6054 | 1635.95 | 16.34164 | 1635.95 | -12.2481 | 1635.95 | 18.79325 | 1635.95 | -97.9917 | 1635.95 | -218.553 |  | 1635.95 | -54.3032 |
| 1636.17 | -15.7528 | 1636.14 | -89.9566 | 1636.58 | 16.18241 | 1636.58 | -14.6004 | 1636.58 | 15.39281 | 1636.58 | -99.7472 | 1636.58 | -221.957 |  | 1636.58 | -54.2588 |
| 1636.81 | -16.0258 | 1636.77 | -90.4254 | 1637.22 | 15.48653 | 1637.22 | -17.2942 | 1637.22 | 12.24396 | 1637.22 | -101.835 | 1637.22 | -225.11 |  | 1637.22 | -54.7477 |
| 1637.45 | -16.2988 | 1637.41 | -90.1066 | 1637.85 | 13.58485 | 1637.85 | -19.132 | 1637.85 | 9.14133 | 1637.85 | -103.075 | 1637.85 | -228.217 |  | 1637.85 | -56.4457 |
| 1638.08 | -16.5713 | 1638.05 | -91.3366 | 1638.49 | 12.40269 | 1638.49 | -18.926 | 1638.49 | 6.48915 | 1638.49 | -102.263 | 1638.49 | -230.873 |  | 1638.49 | -57.421 |
| 1638.72 | -16.8431 | 1638.68 | -91.3307 | 1639.12 | 10.85603 | 1639.12 | -19.7063 | 1639.12 | 2.19373 | 1639.12 | -102.446 | 1639.12 | -235.172 |  | 1639.12 | -58.764 |
| 1639.36 | -17.114 | 1639.32 | -90.1056 | 1639.76 | 10.50026 | 1639.76 | -18.4877 | 1639.76 | -1.23281 | 1639.76 | -100.621 | 1639.76 | -238.603 |  | 1639.76 | -58.9128 |
| 1639.99 | -17.3838 | 1639.96 | -90.3143 | 1640.4 | 10.44918 | 1640.4 | -18.2168 | 1640.4 | -1.9413 | 1640.4 | -99.7441 | 1640.4 | -239.316 |  | 1640.4 | -58.757 |
| 1640.63 | -17.6521 | 1640.6 | -88.6479 | 1641.03 | 10.04263 | 1641.03 | -19.6881 | 1641.03 | -3.32068 | 1641.03 | -100.618 | 1641.03 | -240.699 |  | 1641.03 | -58.9599 |
| 1641.26 | -17.9185 | 1641.23 | -88.334 | 1641.67 | 9.68128 | 1641.67 | -19.1882 | 1641.67 | -4.8402 | 1641.67 | -99.5122 | 1641.67 | -242.223 |  | 1641.67 | -59.1143 |
| 1641.9 | -18.183 | 1641.87 | -88.3503 | 1642.3 | 9.28924 | 1642.3 | -19.9178 | 1642.3 | -4.5188 | 1642.3 | -99.6448 | 1642.3 | -241.905 |  | 1642.3 | -59.3027 |
| 1642.54 | -18.4451 | 1642.51 | -87.6236 | 1642.94 | 8.62082 | 1642.94 | -21.2419 | 1642.94 | -6.45812 | 1642.94 | -100.363 | 1642.94 | -243.849 |  | 1642.94 | -59.7642 |
| 1643.17 | -18.7046 | 1643.14 | -89.5588 | 1643.57 | 7.49536 | 1643.57 | -23.0457 | 1643.57 | -7.57676 | 1643.57 | -101.569 | 1643.57 | -244.971 |  | 1643.57 | -60.686 |
| 1643.81 | -18.9618 | 1643.78 | -90.3444 | 1644.21 | 6.57216 | 1644.21 | -22.7827 | 1644.21 | -7.73769 | 1644.21 | -100.7 | 1644.21 | -245.136 |  | 1644.21 | -61.4023 |
| 1644.44 | -19.2164 | 1644.42 | -90.113 | 1644.84 | 6.10061 | 1644.84 | -22.7326 | 1644.84 | -5.64829 | 1644.84 | -100.053 | 1644.84 | -243.051 |  | 1644.84 | -61.6701 |
| 1645.08 | -19.4685 | 1645.05 | -90.6621 | 1645.48 | 5.19222 | 1645.48 | -22.3216 | 1645.48 | -6.54122 | 1645.48 | -99.0356 | 1645.48 | -243.948 |  | 1645.48 | -62.3716 |
| 1645.71 | -19.7181 | 1645.69 | -92.8397 | 1646.11 | 4.61667 | 1646.11 | -22.5291 | 1646.11 | -8.81559 | 1646.11 | -98.6462 | 1646.11 | -246.226 |  | 1646.11 | -62.7435 |
| 1646.35 | -19.9655 | 1646.33 | -92.9709 | 1646.75 | 5.05573 | 1646.75 | -22.5588 | 1646.75 | -10.8883 | 1646.75 | -98.0695 | 1646.75 | -248.303 |  | 1646.75 | -62.0975 |
| 1646.99 | -20.2107 | 1646.96 | -91.6008 | 1647.38 | 5.08088 | 1647.38 | -21.9057 | 1647.38 | -12.6298 | 1647.38 | -96.8195 | 1647.38 | -250.048 |  | 1647.38 | -61.8687 |
| 1647.62 | -20.4533 | 1647.6 | -92.5329 | 1648.02 | 4.72927 | 1648.02 | -22.6425 | 1648.02 | -12.9651 | 1648.02 | -96.9499 | 1648.02 | -250.388 |  | 1648.02 | -62.0134 |
| 1648.26 | -20.6933 | 1648.24 | -93.1721 | 1648.65 | 4.7403 | 1648.65 | -22.3102 | 1648.65 | -14.584 | 1648.65 | -96.0206 | 1648.65 | -252.011 |  | 1648.65 | -61.7987 |
| 1648.89 | -20.9304 | 1648.87 | -93.9997 | 1649.28 | 5.00427 | 1649.28 | -22.7949 | 1649.28 | -16.4422 | 1649.28 | -95.9084 | 1649.28 | -253.873 |  | 1649.28 | -61.331 |
| 1649.53 | -21.1642 | 1649.51 | -94.1761 | 1649.92 | 3.97668 | 1649.92 | -23.3689 | 1649.92 | -16.844 | 1649.92 | -95.876 | 1649.92 | -254.279 |  | 1649.92 | -62.1517 |
| 1650.16 | -21.3942 | 1650.14 | -93.1439 | 1650.55 | 5.25841 | 1650.55 | -23.8377 | 1650.55 | -17.674 | 1650.55 | -95.748 | 1650.55 | -255.113 |  | 1650.55 | -60.6663 |
| 1650.8 | -21.6205 | 1650.78 | -93.4125 | 1651.19 | 6.25985 | 1651.19 | -23.2896 | 1651.19 | -17.3285 | 1651.19 | -94.5934 | 1651.19 | -254.771 |  | 1651.19 | -59.4579 |
| 1651.43 | -21.843 | 1651.42 | -92.8204 | 1651.82 | 5.72345 | 1651.82 | -22.6015 | 1651.82 | -19.2022 | 1651.82 | -93.3084 | 1651.82 | -256.649 |  | 1651.82 | -59.7907 |
| 1652.07 | -22.0614 | 1652.05 | -91.4335 | 1652.46 | 5.74157 | 1652.46 | -23.3547 | 1652.46 | -20.2444 | 1652.46 | -93.4552 | 1652.46 | -257.695 |  | 1652.46 | -59.5656 |
| 1652.7 | -22.2757 | 1652.69 | -88.7832 | 1653.09 | 5.63929 | 1653.09 | -22.917 | 1653.09 | -20.8039 | 1653.09 | -92.4206 | 1653.09 | -258.259 |  | 1653.09 | -59.4642 |
| 1653.34 | -22.4853 | 1653.32 | -88.195 | 1653.72 | 6.28143 | 1653.72 | -22.7622 | 1653.72 | -21.0357 | 1653.72 | -91.6689 | 1653.72 | -258.495 |  | 1653.72 | -58.6184 |
| 1653.97 | -22.69 | 1653.96 | -88.0295 | 1654.36 | 6.18662 | 1654.36 | -22.4627 | 1654.36 | -19.7271 | 1654.36 | -90.7629 | 1654.36 | -257.19 |  | 1654.36 | -58.5063 |
| 1654.61 | -22.8897 | 1654.59 | -87.7208 | 1654.99 | 6.93514 | 1654.99 | -22.1524 | 1654.99 | -19.0514 | 1654.99 | -89.8557 | 1654.99 | -256.518 |  | 1654.99 | -57.5541 |
| 1655.24 | -23.0846 | 1655.23 | -88.3524 | 1655.63 | 7.41601 | 1655.63 | -22.6089 | 1655.63 | -19.5534 | 1655.63 | -89.7058 | 1655.63 | -257.024 |  | 1655.63 | -56.8663 |
| 1655.88 | -23.2746 | 1655.87 | -88.5781 | 1656.26 | 6.34591 | 1656.26 | -20.6076 | 1656.26 | -20.0883 | 1656.26 | -87.1076 | 1656.26 | -257.563 |  | 1656.26 | -57.7328 |
| 1656.51 | -23.4601 | 1656.5 | -88.4257 | 1656.89 | 5.73964 | 1656.89 | -20.1089 | 1656.89 | -21.0812 | 1656.89 | -86.012 | 1656.89 | -258.56 |  | 1656.89 | -58.1354 |
| 1657.15 | -23.6412 | 1657.14 | -89.5927 | 1657.53 | 4.48641 | 1657.53 | -20.0183 | 1657.53 | -21.0571 | 1657.53 | -85.3149 | 1657.53 | -258.54 |  | 1657.53 | -59.1817 |
| 1657.78 | -23.8179 | 1657.77 | -89.0998 | 1658.16 | 4.0374 | 1658.16 | -19.1401 | 1658.16 | -21.4825 | 1658.16 | -83.8399 | 1658.16 | -258.97 |  | 1658.16 | -59.427 |
| 1658.41 | -23.99 | 1658.41 | -88.9788 | 1658.8 | 3.21065 | 1658.8 | -17.9675 | 1658.8 | -21.6921 | 1658.8 | -82.0609 | 1658.8 | -259.183 |  | 1658.8 | -60.0468 |
| 1659.05 | -24.1576 | 1659.04 | -89.7694 | 1659.43 | 2.50449 | 1659.43 | -17.2186 | 1659.43 | -21.5491 | 1659.43 | -80.715 | 1659.43 | -259.044 |  | 1659.43 | -60.5493 |
| 1659.68 | -24.3208 | 1659.68 | -91.6241 | 1660.06 | 2.90303 | 1660.06 | -17.4041 | 1660.06 | -20.0693 | 1660.06 | -80.3036 | 1660.06 | -257.569 |  | 1660.06 | -59.9471 |
| 1660.32 | -24.4795 | 1660.31 | -93.2885 | 1660.7 | 3.91728 | 1660.7 | -16.2074 | 1660.7 | -19.1539 | 1660.7 | -78.5005 | 1660.7 | -256.657 |  | 1660.7 | -58.7259 |
| 1660.95 | -24.6338 | 1660.95 | -94.4473 | 1661.33 | 4.12857 | 1661.33 | -13.7717 | 1661.33 | -19.1448 | 1661.33 | -75.4679 | 1661.33 | -256.652 |  | 1661.33 | -58.311 |
| 1661.59 | -24.784 | 1661.58 | -95.747 | 1661.96 | 4.34135 | 1661.96 | -12.1567 | 1661.96 | -18.9874 | 1661.96 | -73.256 | 1661.96 | -256.499 |  | 1661.96 | -57.8945 |
| 1662.22 | -24.9301 | 1662.22 | -95.6106 | 1662.6 | 5.51187 | 1662.6 | -11.4756 | 1662.6 | -20.1973 | 1662.6 | -71.9685 | 1662.6 | -257.713 |  | 1662.6 | -56.5171 |
| 1662.85 | -25.0722 | 1662.85 | -93.308 | 1663.23 | 5.99828 | 1663.23 | -11.1399 | 1663.23 | -18.6326 | 1663.23 | -71.0359 | 1663.23 | -256.152 |  | 1663.23 | -55.827 |
| 1663.49 | -25.2102 | 1663.49 | -92.8655 | 1663.86 | 5.94901 | 1663.86 | -10.315 | 1663.86 | -18.1293 | 1663.86 | -69.6141 | 1663.86 | -255.653 |  | 1663.86 | -55.6726 |
| 1664.12 | -25.3438 | 1664.12 | -92.7019 | 1664.5 | 4.7914 | 1664.5 | -10.332 | 1664.5 | -18.0203 | 1664.5 | -69.0246 | 1664.5 | -255.548 |  | 1664.5 | -56.6233 |
| 1664.75 | -25.4725 | 1664.76 | -92.8343 | 1665.13 | 4.2784 | 1665.13 | -10.4033 | 1665.13 | -19.9358 | 1665.13 | -68.4991 | 1665.13 | -257.467 |  | 1665.13 | -56.9326 |
| 1665.39 | -25.596 | 1665.39 | -93.6561 | 1665.76 | 3.51227 | 1665.76 | -10.6308 | 1665.76 | -18.5209 | 1665.76 | -68.1296 | 1665.76 | -256.056 |  | 1665.76 | -57.4951 |
| 1666.02 | -25.7146 | 1666.03 | -93.4856 | 1666.4 | 1.97889 | 1666.4 | -9.64672 | 1666.4 | -15.9594 | 1666.4 | -66.5391 | 1666.4 | -253.499 |  | 1666.4 | -58.8215 |
| 1666.66 | -25.8285 | 1666.66 | -93.2287 | 1667.03 | 0.56659 | 1667.03 | -9.36023 | 1667.03 | -15.7845 | 1667.03 | -65.6557 | 1667.03 | -253.328 |  | 1667.03 | -60.0302 |
| 1667.29 | -25.9372 | 1667.3 | -92.3205 | 1667.66 | -0.10502 | 1667.66 | -8.68861 | 1667.66 | -12.9978 | 1667.66 | -64.3872 | 1667.66 | -250.545 |  | 1667.66 | -60.4981 |
| 1667.92 | -26.0408 | 1667.93 | -91.1936 | 1668.29 | 0.02397 | 1668.29 | -7.87601 | 1668.29 | -11.4391 | 1668.29 | -62.9776 | 1668.29 | -248.991 |  | 1668.29 | -60.1654 |
| 1668.56 | -26.139 | 1668.56 | -90.7705 | 1668.93 | -0.6386 | 1668.93 | -6.79188 | 1668.93 | -9.26268 | 1668.93 | -61.2871 | 1668.93 | -246.818 |  | 1668.93 | -60.6211 |
| 1669.19 | -26.2318 | 1669.2 | -92.7038 | 1669.56 | 0.14646 | 1669.56 | -5.24968 | 1669.56 | -6.10436 | 1669.56 | -59.148 | 1669.56 | -243.664 |  | 1669.56 | -59.6324 |
| 1669.82 | -26.3189 | 1669.83 | -93.0969 | 1670.19 | 0.27407 | 1670.19 | -3.98845 | 1670.19 | -4.78879 | 1670.19 | -57.2898 | 1670.19 | -242.352 |  | 1670.19 | -59.3011 |
| 1670.46 | -26.4001 | 1670.47 | -92.5984 | 1670.82 | 0.03297 | 1670.82 | -3.88524 | 1670.82 | -3.74482 | 1670.82 | -56.5897 | 1670.82 | -241.313 |  | 1670.82 | -59.3385 |
| 1671.09 | -26.4751 | 1671.1 | -91.9001 | 1671.46 | 0.94902 | 1671.46 | -3.67581 | 1671.46 | -1.87981 | 1671.46 | -55.7739 | 1671.46 | -239.452 |  | 1671.46 | -58.2155 |
| 1671.72 | -26.544 | 1671.73 | -90.0662 | 1672.09 | 1.61156 | 1672.09 | -4.8012 | 1672.09 | 0.2296 | 1672.09 | -56.3023 | 1672.09 | -237.346 |  | 1672.09 | -57.3493 |
| 1672.36 | -26.6067 | 1672.37 | -89.6999 | 1672.72 | 1.59429 | 1672.72 | -4.71051 | 1672.72 | 0.12333 | 1672.72 | -55.6147 | 1672.72 | -237.456 |  | 1672.72 | -57.1629 |
| 1672.99 | -26.6635 | 1673 | -89.9362 | 1673.35 | 1.93349 | 1673.35 | -3.77903 | 1673.35 | 0 | 1673.35 | -54.0863 | 1673.35 | -237.584 |  | 1673.35 | -56.62 |
| 1673.62 | -26.714 | 1673.64 | -89.6048 | 1673.99 | 1.46408 | 1673.99 | -3.58406 | 1673.99 | -2.13187 | 1673.99 | -53.285 | 1673.99 | -238.298 |  | 1673.99 | -56.8825 |
| 1674.25 | -26.7585 | 1674.27 | -89.718 | 1674.62 | -0.10485 | 1674.62 | -3.53706 | 1674.62 | -5.99179 | 1674.62 | -52.641 | 1674.62 | -240.762 |  | 1674.62 | -58.2478 |
| 1674.89 | -26.7972 | 1674.9 | -90.4982 | 1675.25 | -1.85994 | 1675.25 | -1.92494 | 1675.25 | -8.81665 | 1675.25 | -50.432 | 1675.25 | -242.191 |  | 1675.25 | -59.7992 |
| 1675.52 | -26.8301 | 1675.54 | -89.2746 | 1675.88 | -1.75424 | 1675.88 | -1.25282 | 1675.88 | -11.3537 | 1675.88 | -49.163 | 1675.88 | -243.333 |  | 1675.88 | -59.4898 |
| 1676.15 | -26.8575 | 1676.17 | -88.6406 | 1676.51 | -1.48776 | 1676.51 | -1.58207 | 1676.51 | -14.4938 | 1676.51 | -48.8953 | 1676.51 | -245.077 |  | 1676.51 | -59.0197 |
| 1676.79 | -26.8798 | 1676.8 | -87.0816 | 1677.15 | -2.11539 | 1677.15 | -0.84057 | 1677.15 | -17.9636 | 1677.15 | -47.5474 | 1677.15 | -247.129 |  | 1677.15 | -59.4404 |
| 1677.42 | -26.8969 | 1677.44 | -87.4523 | 1677.78 | -2.2074 | 1677.78 | 0.15951 | 1677.78 | -21.356 | 1677.78 | -45.9504 | 1677.78 | -249.126 |  | 1677.78 | -59.3287 |
| 1678.05 | -26.9089 | 1678.07 | -87.3509 | 1678.41 | 0 | 1678.41 | -0.131 | 1678.41 | -21.9697 | 1678.41 | -45.644 | 1678.41 | -248.344 |  | 1678.41 | -56.9176 |
| 1678.68 | -26.9159 | 1678.7 | -88.7781 | 1679.04 | -1.00224 | 1679.04 | 0.78675 | 1679.04 | -25.0562 | 1679.04 | -44.1293 | 1679.04 | -250.035 |  | 1679.04 | -57.6917 |
| 1679.31 | -26.9178 | 1679.34 | -88.8013 | 1679.67 | -0.74114 | 1679.67 | 0 | 1679.67 | -29.0046 | 1679.67 | -44.3191 | 1679.67 | -252.587 |  | 1679.67 | -57.2025 |
| 1679.95 | -26.9151 | 1679.97 | -86.243 | 1680.31 | -0.92201 | 1680.31 | -0.22566 | 1680.31 | -28.5742 | 1680.31 | -44.3762 | 1680.31 | -250.739 |  | 1680.31 | -57.1516 |
| 1680.58 | -26.9089 | 1680.6 | -87.41 | 1680.94 | -1.30111 | 1680.94 | -0.00552 | 1680.94 | -31.9517 | 1680.94 | -43.9902 | 1680.94 | -252.721 |  | 1680.94 | -57.3026 |
| 1681.21 | -26.8989 | 1681.24 | -86.858 | 1681.57 | -1.81825 | 1681.57 | 0.82482 | 1681.57 | -33.8998 | 1681.57 | -42.9939 | 1681.57 | -253.273 |  | 1681.57 | -57.5916 |
| 1681.84 | -26.8854 | 1681.87 | -86.6722 | 1682.2 | -1.365 | 1682.2 | 1.77555 | 1682.2 | -37.4925 | 1682.2 | -41.8773 | 1682.2 | -255.47 |  | 1682.2 | -56.9102 |
| 1682.48 | -26.8677 | 1682.5 | -87.0366 | 1682.83 | -2.17321 | 1682.83 | 1.30435 | 1682.83 | -38.6696 | 1682.83 | -42.1826 | 1682.83 | -255.252 |  | 1682.83 | -57.4903 |
| 1683.11 | -26.8457 | 1683.14 | -84.9078 | 1683.46 | -1.59004 | 1683.46 | -0.73019 | 1683.46 | -40.9054 | 1683.46 | -44.0512 | 1683.46 | -256.092 |  | 1683.46 | -56.679 |
| 1683.74 | -26.8195 | 1683.77 | -87.2825 | 1684.09 | -2.77354 | 1684.09 | -0.13217 | 1684.09 | -43.2268 | 1684.09 | -43.2873 | 1684.09 | -257.018 |  | 1684.09 | -57.6344 |
| 1684.37 | -26.7888 | 1684.4 | -87.7811 | 1684.72 | -3.19225 | 1684.72 | 0.36522 | 1684.72 | -45.6531 | 1684.72 | -42.624 | 1684.72 | -258.048 |  | 1684.72 | -57.825 |
| 1685 | -26.7534 | 1685.03 | -87.0594 | 1685.36 | -3.69506 | 1685.36 | 1.87766 | 1685.36 | -46.5601 | 1685.36 | -40.943 | 1685.36 | -257.537 |  | 1685.36 | -58.096 |
| 1685.63 | -26.7131 | 1685.67 | -87.9466 | 1685.99 | -4.32425 | 1685.99 | 3.15646 | 1685.99 | -50.5713 | 1685.99 | -39.4983 | 1685.99 | -260.153 |  | 1685.99 | -58.4971 |
| 1686.27 | -26.6677 | 1686.3 | -88.1499 | 1686.62 | -4.06069 | 1686.62 | 3.02702 | 1686.62 | -53.8247 | 1686.62 | -39.4618 | 1686.62 | -262.011 |  | 1686.62 | -58.0054 |
| 1686.9 | -26.6166 | 1686.93 | -90.4544 | 1687.25 | -6.00576 | 1687.25 | 1.57464 | 1687.25 | -57.1924 | 1687.25 | -40.7483 | 1687.25 | -263.983 |  | 1687.25 | -59.7223 |
| 1687.53 | -26.5601 | 1687.56 | -88.7588 | 1687.88 | -6.47523 | 1687.88 | 2.02582 | 1687.88 | -57.6427 | 1687.88 | -40.1312 | 1687.88 | -263.037 |  | 1687.88 | -59.9637 |
| 1688.16 | -26.4985 | 1688.2 | -88.5508 | 1688.51 | -6.32666 | 1688.51 | 2.53209 | 1688.51 | -59.7505 | 1688.51 | -39.459 | 1688.51 | -263.749 |  | 1688.51 | -59.587 |
| 1688.79 | -26.4316 | 1688.83 | -87.649 | 1689.14 | -6.99055 | 1689.14 | 4.02089 | 1689.14 | -57.9741 | 1689.14 | -37.8043 | 1689.14 | -260.577 |  | 1689.14 | -60.0227 |
| 1689.42 | -26.36 | 1689.46 | -88.2601 | 1689.77 | -8.65719 | 1689.77 | 5.80067 | 1689.77 | -57.8443 | 1689.77 | -35.8586 | 1689.77 | -259.052 |  | 1689.77 | -61.4612 |
| 1690.06 | -26.2834 | 1690.09 | -89.0321 | 1690.4 | -8.19078 | 1690.4 | 6.36204 | 1690.4 | -55.3601 | 1690.4 | -35.1314 | 1690.4 | -255.172 |  | 1690.4 | -60.7667 |
| 1690.69 | -26.2019 | 1690.73 | -88.4783 | 1691.03 | -8.56241 | 1691.03 | 7.52754 | 1691.03 | -55.2604 | 1691.03 | -33.8 | 1691.03 | -253.677 |  | 1691.03 | -60.9102 |
| 1691.32 | -26.1154 | 1691.36 | -88.4909 | 1691.66 | -7.31482 | 1691.66 | 7.35793 | 1691.66 | -53.7072 | 1691.66 | -33.8037 | 1691.66 | -250.728 |  | 1691.66 | -59.4345 |
| 1691.95 | -26.0239 | 1691.99 | -88.4105 | 1692.29 | -7.69292 | 1692.29 | 8.21087 | 1692.29 | -52.961 | 1692.29 | -32.7848 | 1692.29 | -248.586 |  | 1692.29 | -59.5844 |
| 1692.58 | -25.9274 | 1692.62 | -87.2695 | 1692.92 | -8.342 | 1692.92 | 10.54185 | 1692.92 | -52.1872 | 1692.92 | -30.2879 | 1692.92 | -246.416 |  | 1692.92 | -60.0054 |
| 1693.21 | -25.8261 | 1693.25 | -87.3767 | 1693.17 | -7.52866 | 1693.17 | 12.41941 | 1693.17 | -49.6455 | 1693.17 | -28.3445 | 1693.17 | -243.321 |  | 1693.17 | -59.1015 |
| 1693.84 | -25.7201 | 1693.89 | -87.6844 | 1693.8 | -6.31547 | 1693.8 | 13.63571 | 1693.8 | -50.6084 | 1693.8 | -26.9623 | 1693.8 | -242.888 |  | 1693.8 | -57.6602 |
| 1694.47 | -25.6092 | 1694.52 | -88.9173 | 1694.43 | -6.23503 | 1694.43 | 13.93555 | 1694.43 | -48.539 | 1694.43 | -26.4966 | 1694.43 | -239.423 |  | 1694.43 | -57.3516 |
| 1695.1 | -25.4937 | 1695.15 | -88.4913 | 1695.06 | -5.20086 | 1695.06 | 13.80597 | 1695.06 | -49.9142 | 1695.06 | -26.4602 | 1695.06 | -239.402 |  | 1695.06 | -56.0893 |
| 1695.74 | -25.3732 | 1695.78 | -90.1707 | 1695.7 | -4.21816 | 1695.7 | 15.95591 | 1695.7 | -49.4049 | 1695.7 | -24.1417 | 1695.7 | -237.475 |  | 1695.7 | -54.8749 |
| 1696.37 | -25.2478 | 1696.41 | -90.1675 | 1696.33 | -0.78368 | 1696.33 | 17.10244 | 1696.33 | -47.0824 | 1696.33 | -22.8293 | 1696.33 | -233.757 |  | 1696.33 | -51.2123 |
| 1697 | -25.1175 | 1697.04 | -89.9225 | 1696.96 | 1.55264 | 1696.96 | 19.34169 | 1696.96 | -45.661 | 1696.96 | -20.4241 | 1696.96 | -230.94 |  | 1696.96 | -48.6478 |
| 1697.63 | -24.9823 | 1697.68 | -90.9042 | 1697.59 | 2.89034 | 1697.59 | 20.90603 | 1697.59 | -46.0084 | 1697.59 | -18.6939 | 1697.59 | -229.892 |  | 1697.59 | -47.082 |
| 1698.26 | -24.8419 | 1698.31 | -90.2283 | 1698.22 | 6.28059 | 1698.22 | 21.33783 | 1698.22 | -45.1658 | 1698.22 | -18.0962 | 1698.22 | -227.654 |  | 1698.22 | -43.4636 |
| 1698.89 | -24.6968 | 1698.94 | -91.3751 | 1698.85 | 8.57691 | 1698.85 | 22.48452 | 1698.85 | -41.8973 | 1698.85 | -16.7836 | 1698.85 | -222.989 |  | 1698.85 | -40.9392 |
| 1699.52 | -24.5467 | 1699.57 | -91.482 | 1699.48 | 9.48461 | 1699.48 | 22.38808 | 1699.48 | -41.3006 | 1699.48 | -16.7141 | 1699.48 | -220.997 |  | 1699.48 | -39.8033 |
| 1700.15 | -24.3914 | 1700.2 | -91.3794 | 1700.12 | 9.49947 | 1700.12 | 23.6992 | 1700.12 | -40.5048 | 1700.12 | -15.2345 | 1700.12 | -218.783 |  | 1700.12 | -39.5567 |
| 1700.78 | -24.2311 | 1700.83 | -90.1145 | 1700.75 | 11.31815 | 1700.75 | 24.38041 | 1700.75 | -38.4554 | 1700.75 | -14.3873 | 1700.75 | -215.338 |  | 1700.75 | -37.5099 |
| 1701.41 | -24.0658 | 1701.46 | -89.9986 | 1701.38 | 11.53242 | 1701.38 | 25.87615 | 1701.38 | -39.2393 | 1701.38 | -12.7257 | 1701.38 | -214.726 |  | 1701.38 | -37.0675 |
| 1702.04 | -23.8955 | 1702.09 | -91.5199 | 1702.01 | 12.38925 | 1702.01 | 28.51405 | 1702.01 | -40.3818 | 1702.01 | -9.92187 | 1702.01 | -214.473 |  | 1702.01 | -35.9825 |
| 1702.67 | -23.7199 | 1702.73 | -91.8523 | 1702.64 | 12.87784 | 1702.64 | 28.62941 | 1702.64 | -40.0036 | 1702.64 | -9.64061 | 1702.64 | -212.699 |  | 1702.64 | -35.2658 |
| 1703.3 | -23.5393 | 1703.36 | -92.128 | 1703.27 | 12.92467 | 1703.27 | 30.75672 | 1703.27 | -39.5418 | 1703.27 | -7.34739 | 1703.27 | -210.842 |  | 1703.27 | -34.9909 |
| 1703.93 | -23.3533 | 1703.99 | -92.0532 | 1703.9 | 11.92278 | 1703.9 | 32.33151 | 1703.9 | -39.7124 | 1703.9 | -5.60669 | 1703.9 | -209.617 |  | 1703.9 | -35.7646 |
| 1704.56 | -23.1618 | 1704.62 | -91.3114 | 1704.54 | 13.04069 | 1704.54 | 34.07462 | 1704.54 | -36.9222 | 1704.54 | -3.69503 | 1704.54 | -205.409 |  | 1704.54 | -34.415 |
| 1705.19 | -22.9636 | 1705.25 | -91.1906 | 1705.17 | 13.82351 | 1705.17 | 34.16334 | 1705.17 | -35.3815 | 1705.17 | -3.44041 | 1705.17 | -202.472 |  | 1705.17 | -33.404 |
| 1705.82 | -22.7599 | 1705.88 | -90.0186 | 1705.8 | 14.78377 | 1705.8 | 33.58283 | 1705.8 | -34.9315 | 1705.8 | -3.855 | 1705.8 | -200.627 |  | 1705.8 | -32.2156 |
| 1706.45 | -22.5511 | 1706.51 | -91.4515 | 1706.43 | 16.44169 | 1706.43 | 34.98508 | 1706.43 | -31.5113 | 1706.43 | -2.28685 | 1706.43 | -195.811 |  | 1706.43 | -30.3296 |
| 1707.08 | -22.3372 | 1707.14 | -90.5544 | 1707.06 | 18.85255 | 1707.06 | 36.57026 | 1707.06 | -28.6969 | 1707.06 | -0.53576 | 1707.06 | -191.601 |  | 1707.06 | -27.6906 |
| 1707.71 | -22.1184 | 1707.77 | -90.9971 | 1707.69 | 19.20772 | 1707.69 | 37.42348 | 1707.69 | -28.0592 | 1707.69 | 0.48337 | 1707.69 | -189.568 |  | 1707.69 | -27.1073 |
| 1708.34 | -21.8953 | 1708.4 | -91.3639 | 1708.32 | 19.81191 | 1708.32 | 38.2071 | 1708.32 | -26.0967 | 1708.32 | 1.4329 | 1708.32 | -186.209 |  | 1708.32 | -26.275 |
| 1708.97 | -21.6686 | 1709.03 | -92.0083 | 1708.95 | 21.44374 | 1708.95 | 38.91777 | 1708.95 | -23.5417 | 1708.95 | 2.30948 | 1708.95 | -182.259 |  | 1708.95 | -24.415 |
| 1709.6 | -21.4387 | 1709.66 | -91.4903 | 1709.58 | 22.35359 | 1709.58 | 40.24993 | 1709.58 | -21.4086 | 1709.58 | 3.80755 | 1709.58 | -178.73 |  | 1709.58 | -23.277 |
| 1710.23 | -21.2059 | 1710.29 | -91.6963 | 1710.21 | 21.24677 | 1710.21 | 40.95071 | 1710.21 | -20.5555 | 1710.21 | 4.67424 | 1710.21 | -176.481 |  | 1710.21 | -24.1557 |
| 1710.86 | -20.9707 | 1710.92 | -93.4776 | 1710.84 | 22.43858 | 1710.84 | 42.29659 | 1710.84 | -19.793 | 1710.84 | 6.18603 | 1710.84 | -174.323 |  | 1710.84 | -22.7358 |
| 1711.48 | -20.733 | 1711.55 | -92.9583 | 1711.47 | 22.61824 | 1711.47 | 43.64228 | 1711.47 | -15.8148 | 1711.47 | 7.69762 | 1711.47 | -168.949 |  | 1711.47 | -22.328 |
| 1712.11 | -20.4931 | 1712.18 | -92.8616 | 1712.1 | 23.87937 | 1712.1 | 45.59642 | 1712.1 | -16.8372 | 1712.1 | 9.81768 | 1712.1 | -168.576 |  | 1712.1 | -20.8387 |
| 1712.74 | -20.2521 | 1712.81 | -93.0181 | 1712.74 | 25.02954 | 1712.74 | 46.69365 | 1712.74 | -13.7576 | 1712.74 | 11.08344 | 1712.74 | -164.078 |  | 1712.74 | -19.4568 |
| 1713.37 | -20.0106 | 1713.44 | -91.7445 | 1713.37 | 26.10627 | 1713.37 | 47.56135 | 1713.37 | -12.731 | 1713.37 | 12.11705 | 1713.37 | -161.656 |  | 1713.37 | -18.1519 |
| 1714 | -19.7686 | 1714.07 | -92.1856 | 1714 | 27.42654 | 1714 | 47.52454 | 1714 | -10.2261 | 1714 | 12.24616 | 1714 | -157.755 |  | 1714 | -16.6035 |
| 1714.63 | -19.526 | 1714.7 | -93.7207 | 1714.63 | 28.36504 | 1714.63 | 50.54479 | 1714.63 | -8.50991 | 1714.63 | 15.43232 | 1714.63 | -154.644 |  | 1714.63 | -15.4369 |
| 1715.26 | -19.2827 | 1715.33 | -91.7512 | 1715.26 | 30.99765 | 1715.26 | 53.24759 | 1715.26 | -10.5289 | 1715.26 | 18.30102 | 1715.26 | -155.267 |  | 1715.26 | -12.5762 |
| 1715.89 | -19.0389 | 1715.96 | -90.4576 | 1715.89 | 33.33635 | 1715.89 | 52.57412 | 1715.89 | -8.06742 | 1715.89 | 17.79346 | 1715.89 | -151.41 |  | 1715.89 | -10.0093 |
| 1716.52 | -18.795 | 1716.59 | -90.3137 | 1716.52 | 34.53887 | 1716.52 | 53.51655 | 1716.52 | -6.92563 | 1716.52 | 18.9018 | 1716.52 | -148.872 |  | 1716.52 | -8.57867 |
| 1717.15 | -18.5508 | 1717.22 | -89.783 | 1717.15 | 35.68877 | 1717.15 | 52.92843 | 1717.15 | -6.00408 | 1717.15 | 18.47959 | 1717.15 | -146.555 |  | 1717.15 | -7.20065 |
| 1717.77 | -18.3065 | 1717.85 | -88.9926 | 1717.78 | 35.51591 | 1717.78 | 52.32089 | 1717.78 | -2.92468 | 1717.78 | 18.03796 | 1717.78 | -142.08 |  | 1717.78 | -7.14537 |
| 1718.4 | -18.0621 | 1718.48 | -88.8702 | 1718.41 | 35.72914 | 1718.41 | 52.24218 | 1718.41 | -2.18568 | 1718.41 | 18.12516 | 1718.41 | -139.945 |  | 1718.41 | -6.70401 |
| 1719.03 | -17.8179 | 1719.11 | -89.1259 | 1719.04 | 38.37648 | 1719.04 | 54.56582 | 1719.04 | -1.12001 | 1719.04 | 20.61471 | 1719.04 | -137.484 |  | 1719.04 | -3.82854 |
| 1719.66 | -17.574 | 1719.74 | -89.0045 | 1719.66 | 37.88745 | 1719.66 | 55.63112 | 1719.66 | -0.26238 | 1719.66 | 21.84328 | 1719.66 | -135.253 |  | 1719.66 | -4.09306 |
| 1720.29 | -17.3304 | 1720.37 | -88.4364 | 1720.3 | 39.6845 | 1720.3 | 55.54036 | 1720.3 | -0.54396 | 1720.3 | 21.92106 | 1720.3 | -134.117 |  | 1720.3 | -2.06426 |
| 1720.92 | -17.0876 | 1721 | -89.4973 | 1720.92 | 40.5602 | 1720.92 | 54.73296 | 1720.92 | -1.23563 | 1720.92 | 21.27694 | 1720.92 | -133.435 |  | 1720.92 | -0.96405 |
| 1721.54 | -16.8459 | 1721.63 | -87.3796 | 1721.55 | 43.94403 | 1721.55 | 54.57764 | 1721.55 | -1.45259 | 1721.55 | 21.28753 | 1721.55 | -132.256 |  | 1721.55 | 2.64791 |
| 1722.17 | -16.6055 | 1722.26 | -88.0763 | 1722.18 | 44.08532 | 1722.18 | 54.98212 | 1722.18 | -3.63347 | 1722.18 | 21.85792 | 1722.18 | -133.041 |  | 1722.18 | 3.01733 |
| 1722.8 | -16.3663 | 1722.89 | -88.0308 | 1722.81 | 45.29484 | 1722.81 | 54.52611 | 1722.81 | -2.0969 | 1722.81 | 21.56782 | 1722.81 | -130.109 |  | 1722.81 | 4.45498 |
| 1723.43 | -16.1283 | 1723.51 | -87.5247 | 1723.44 | 44.98186 | 1723.44 | 56.13413 | 1723.44 | -4.48935 | 1723.44 | 23.34175 | 1723.44 | -131.106 |  | 1723.44 | 4.37013 |
| 1724.06 | -15.8915 | 1724.14 | -88.1165 | 1724.07 | 45.34809 | 1724.07 | 56.95292 | 1724.07 | -3.95753 | 1724.07 | 24.32644 | 1724.07 | -129.178 |  | 1724.07 | 4.96449 |
| 1724.69 | -15.6562 | 1724.77 | -87.6034 | 1724.7 | 45.74338 | 1724.7 | 56.68612 | 1724.7 | -5.37218 | 1724.7 | 24.22556 | 1724.7 | -129.197 |  | 1724.7 | 5.58791 |
| 1725.31 | -15.4227 | 1725.4 | -88.0536 | 1725.33 | 45.63304 | 1725.33 | 56.81688 | 1725.33 | -7.46369 | 1725.33 | 24.52222 | 1725.33 | -129.893 |  | 1725.33 | 5.7057 |
| 1725.94 | -15.1913 | 1726.03 | -89.3359 | 1725.96 | 45.1294 | 1725.96 | 56.9293 | 1725.96 | -6.09853 | 1725.96 | 24.80056 | 1725.96 | -127.132 |  | 1725.96 | 5.4302 |
| 1726.57 | -14.9624 | 1726.66 | -90.018 | 1726.59 | 44.95184 | 1726.59 | 57.57329 | 1726.59 | -6.50047 | 1726.59 | 25.61045 | 1726.59 | -126.138 |  | 1726.59 | 5.48076 |
| 1727.2 | -14.7357 | 1727.29 | -91.1834 | 1727.22 | 45.2206 | 1727.22 | 57.37776 | 1727.22 | -5.13751 | 1727.22 | 25.58083 | 1727.22 | -123.38 |  | 1727.22 | 5.97765 |
| 1727.82 | -14.5118 | 1727.92 | -90.4728 | 1727.85 | 46.06999 | 1727.85 | 55.81665 | 1727.85 | -2.70573 | 1727.85 | 24.18563 | 1727.85 | -119.552 |  | 1727.85 | 7.05517 |
| 1728.45 | -14.2904 | 1728.55 | -91.0617 | 1728.47 | 43.68011 | 1728.47 | 55.39651 | 1728.47 | -3.81349 | 1728.47 | 23.92877 | 1728.47 | -119.287 |  | 1728.47 | 4.8898 |
| 1729.08 | -14.0717 | 1729.17 | -92.1546 | 1729.1 | 42.22749 | 1729.1 | 54.79611 | 1729.1 | -4.0695 | 1729.1 | 23.49427 | 1729.1 | -118.147 |  | 1729.1 | 3.66531 |
| 1729.71 | -13.8562 | 1729.8 | -93.0131 | 1729.73 | 44.17453 | 1729.73 | 55.60188 | 1729.73 | -3.50544 | 1729.73 | 24.46595 | 1729.73 | -116.187 |  | 1729.73 | 5.84048 |
| 1730.33 | -13.6443 | 1730.43 | -93.4888 | 1730.36 | 44.09259 | 1730.36 | 57.27619 | 1730.36 | -3.47326 | 1730.36 | 26.30617 | 1730.36 | -114.759 |  | 1730.36 | 5.98668 |
| 1730.96 | -13.4359 | 1731.06 | -93.1315 | 1730.99 | 43.06437 | 1730.99 | 57.01205 | 1730.99 | -5.26813 | 1730.99 | 26.20794 | 1730.99 | -115.159 |  | 1730.99 | 5.18659 |
| 1731.59 | -13.2315 | 1731.69 | -91.5447 | 1731.62 | 43.54561 | 1731.62 | 57.70331 | 1731.62 | -4.29194 | 1731.62 | 27.06511 | 1731.62 | -112.787 |  | 1731.62 | 5.89595 |
| 1732.22 | -13.0297 | 1732.32 | -93.1755 | 1732.25 | 44.51415 | 1732.25 | 56.66624 | 1732.25 | -1.74901 | 1732.25 | 26.19395 | 1732.25 | -108.848 |  | 1732.25 | 7.09262 |
| 1732.84 | -12.8308 | 1732.94 | -92.9 | 1732.87 | 44.07087 | 1732.87 | 58.23308 | 1732.87 | -2.5415 | 1732.87 | 27.92407 | 1732.87 | -108.267 |  | 1732.87 | 6.87385 |
| 1733.47 | -12.6349 | 1733.57 | -92.3981 | 1733.5 | 44.6465 | 1733.5 | 57.14316 | 1733.5 | -2.35064 | 1733.5 | 27.00005 | 1733.5 | -106.68 |  | 1733.5 | 7.67762 |
| 1734.1 | -12.4422 | 1734.2 | -92.4066 | 1734.13 | 46.65297 | 1734.13 | 54.22294 | 1734.13 | -1.88323 | 1734.13 | 24.24575 | 1734.13 | -104.817 |  | 1734.13 | 9.91222 |
| 1734.72 | -12.2527 | 1734.83 | -92.5299 | 1734.76 | 46.87556 | 1734.76 | 54.32263 | 1734.76 | -0.74163 | 1734.76 | 24.51135 | 1734.76 | -102.28 |  | 1734.76 | 10.36294 |
| 1735.35 | -12.0665 | 1735.46 | -93.6701 | 1735.39 | 47.50932 | 1735.39 | 54.92035 | 1735.39 | 0.46096 | 1735.39 | 25.27497 | 1735.39 | -99.6818 |  | 1735.39 | 11.22483 |
| 1735.98 | -11.8836 | 1736.08 | -92.7841 | 1736.02 | 49.57341 | 1736.02 | 54.36422 | 1736.02 | 0.71289 | 1736.02 | 24.88475 | 1736.02 | -98.0342 |  | 1736.02 | 13.51705 |
| 1736.6 | -11.7038 | 1736.71 | -93.6598 | 1736.64 | 49.49442 | 1736.64 | 53.75399 | 1736.64 | -1.04515 | 1736.64 | 24.43779 | 1736.64 | -98.4188 |  | 1736.64 | 13.66256 |
| 1737.23 | -11.5272 | 1737.34 | -94.252 | 1737.27 | 49.93834 | 1737.27 | 54.3552 | 1737.27 | -1.22608 | 1737.27 | 25.20492 | 1737.27 | -97.204 |  | 1737.27 | 14.33462 |
| 1737.86 | -11.3535 | 1737.97 | -94.0656 | 1737.9 | 50.32075 | 1737.9 | 56.13201 | 1737.9 | -0.83281 | 1737.9 | 27.14763 | 1737.9 | -95.4151 |  | 1737.9 | 14.94516 |
| 1738.49 | -11.1827 | 1738.59 | -96.3179 | 1738.53 | 51.88883 | 1738.53 | 55.69311 | 1738.53 | -1.88992 | 1738.53 | 26.87464 | 1738.53 | -95.0765 |  | 1738.53 | 16.74137 |
| 1739.11 | -11.015 | 1739.22 | -94.1161 | 1739.16 | 51.85775 | 1739.16 | 55.25451 | 1739.16 | -1.43146 | 1739.16 | 26.60196 | 1739.16 | -93.2223 |  | 1739.16 | 16.93841 |
| 1739.74 | -10.8501 | 1739.85 | -94.4408 | 1739.78 | 51.83798 | 1739.78 | 54.20551 | 1739.78 | 1.41256 | 1739.78 | 25.71623 | 1739.78 | -89.0048 |  | 1739.78 | 17.14315 |
| 1740.37 | -10.6883 | 1740.48 | -94.5883 | 1740.41 | 53.87104 | 1740.41 | 54.86014 | 1740.41 | 0.83366 | 1740.41 | 26.53677 | 1740.41 | -88.188 |  | 1740.41 | 19.40435 |
| 1740.99 | -10.5296 | 1741.1 | -94.6516 | 1741.04 | 53.77534 | 1741.04 | 55.56624 | 1741.04 | -0.09125 | 1741.04 | 27.40878 | 1741.04 | -87.7173 |  | 1741.04 | 19.53677 |
| 1741.62 | -10.3741 | 1741.73 | -93.8583 | 1741.67 | 54.35575 | 1741.67 | 54.65421 | 1741.67 | -1.07824 | 1741.67 | 26.66266 | 1741.67 | -87.3086 |  | 1741.67 | 20.34532 |
| 1742.24 | -10.2223 | 1742.36 | -93.8265 | 1742.29 | 54.67272 | 1742.29 | 56.61794 | 1742.29 | -0.94051 | 1742.29 | 28.78966 | 1742.29 | -85.7973 |  | 1742.29 | 20.8868 |
| 1742.87 | -10.0743 | 1742.99 | -93.7787 | 1742.92 | 54.57161 | 1742.92 | 56.31247 | 1742.92 | 0.44122 | 1742.92 | 28.6501 | 1742.92 | -83.0199 |  | 1742.92 | 21.01382 |
| 1743.5 | -9.93028 | 1743.61 | -92.6163 | 1743.55 | 55.75401 | 1743.55 | 56.25365 | 1743.55 | 0.4665 | 1743.55 | 28.75719 | 1743.55 | -81.599 |  | 1743.55 | 22.42435 |
| 1744.12 | -9.79025 | 1744.24 | -92.1838 | 1744.18 | 57.37391 | 1744.18 | 56.04474 | 1744.18 | 0.51067 | 1744.18 | 28.71418 | 1744.18 | -80.1591 |  | 1744.18 | 24.27238 |
| 1744.75 | -9.65448 | 1744.87 | -93.1714 | 1744.8 | 58.60737 | 1744.8 | 55.69343 | 1744.8 | 1.17398 | 1744.8 | 28.52616 | 1744.8 | -78.1223 |  | 1744.8 | 25.73035 |
| 1745.37 | -9.52347 | 1745.49 | -92.8342 | 1745.43 | 59.80112 | 1745.43 | 56.30203 | 1745.43 | 2.39632 | 1745.43 | 29.30066 | 1745.43 | -75.5043 |  | 1745.43 | 27.15223 |
| 1746 | -9.39722 | 1746.12 | -92.1308 | 1746.06 | 60.08315 | 1746.06 | 57.8774 | 1746.06 | 3.02011 | 1746.06 | 31.04194 | 1746.06 | -73.4848 |  | 1746.06 | 27.66239 |
| 1746.63 | -9.2756 | 1746.75 | -92.0979 | 1746.68 | 61.42801 | 1746.68 | 58.48617 | 1746.68 | 3.87764 | 1746.68 | 31.81399 | 1746.68 | -71.2537 |  | 1746.68 | 29.23176 |
| 1747.25 | -9.15858 | 1747.37 | -92.45 | 1747.31 | 59.834 | 1747.31 | 58.60378 | 1747.31 | 10.43212 | 1747.31 | 32.09751 | 1747.31 | -63.3036 |  | 1747.31 | 27.86588 |
| 1747.88 | -9.04602 | 1748 | -92.1925 | 1747.94 | 59.82821 | 1747.94 | 59.46177 | 1747.94 | 11.67465 | 1747.94 | 33.12141 | 1747.94 | -60.6654 |  | 1747.94 | 28.08822 |
| 1748.5 | -8.93778 | 1748.63 | -94.2199 | 1748.57 | 59.34169 | 1748.57 | 60.54183 | 1748.57 | 14.1898 | 1748.57 | 34.36737 | 1748.57 | -56.7546 |  | 1748.57 | 27.82983 |
| 1749.13 | -8.83376 | 1749.25 | -93.7353 | 1749.19 | 60.45161 | 1749.19 | 62.41585 | 1749.19 | 14.96402 | 1749.19 | 36.40467 | 1749.19 | -54.6068 |  | 1749.19 | 29.16426 |
| 1749.76 | -8.73356 | 1749.88 | -94.1026 | 1749.82 | 63.1858 | 1749.82 | 63.58773 | 1749.82 | 15.26617 | 1749.82 | 37.74246 | 1749.82 | -52.909 |  | 1749.82 | 32.12658 |
| 1750.38 | -8.63726 | 1750.51 | -94.1867 | 1750.45 | 64.42703 | 1750.45 | 65.99273 | 1750.45 | 17.25618 | 1750.45 | 40.31337 | 1750.45 | -49.5233 |  | 1750.45 | 33.59594 |
| 1751.01 | -8.54478 | 1751.13 | -93.7153 | 1751.07 | 64.77586 | 1751.07 | 66.11577 | 1751.07 | 18.07567 | 1751.07 | 40.59968 | 1751.07 | -47.3303 |  | 1751.07 | 34.16928 |
| 1751.63 | -8.45602 | 1751.76 | -93.6037 | 1751.7 | 67.4864 | 1751.7 | 66.11862 | 1751.7 | 16.96543 | 1751.7 | 40.76844 | 1751.7 | -47.0448 |  | 1751.7 | 37.10795 |
| 1752.26 | -8.37099 | 1752.38 | -93.2814 | 1752.33 | 67.00399 | 1752.33 | 66.5895 | 1752.33 | 18.7309 | 1752.33 | 41.40523 | 1752.33 | -43.8837 |  | 1752.33 | 36.85367 |
| 1752.88 | -8.28963 | 1753.01 | -95.3164 | 1752.95 | 68.31554 | 1752.95 | 67.8325 | 1752.95 | 19.49726 | 1752.95 | 42.81151 | 1752.95 | -41.7438 |  | 1752.95 | 38.38973 |
| 1753.51 | -8.21207 | 1753.64 | -95.9363 | 1753.58 | 68.41835 | 1753.58 | 69.53128 | 1753.58 | 21.41561 | 1753.58 | 44.6762 | 1753.58 | -38.4298 |  | 1753.58 | 38.72067 |
| 1754.13 | -8.13792 | 1754.26 | -95.9528 | 1754.2 | 70.18385 | 1754.2 | 70.59986 | 1754.2 | 23.83716 | 1754.2 | 45.90805 | 1754.2 | -34.6347 |  | 1754.2 | 40.71068 |
| 1754.76 | -8.0673 | 1754.89 | -96.4136 | 1754.83 | 70.6271 | 1754.83 | 70.57805 | 1754.83 | 24.09991 | 1754.83 | 46.05215 | 1754.83 | -32.9763 |  | 1754.83 | 41.38205 |
| 1755.38 | -7.9995 | 1755.52 | -95.5385 | 1755.46 | 70.98185 | 1755.46 | 70.9971 | 1755.46 | 25.11739 | 1755.46 | 46.63711 | 1755.46 | -30.5631 |  | 1755.46 | 41.96494 |
| 1756.01 | -7.9341 | 1756.14 | -96.0086 | 1756.08 | 72.70106 | 1756.08 | 71.71752 | 1756.08 | 24.3983 | 1756.08 | 47.52081 | 1756.08 | -29.9087 |  | 1756.08 | 43.90866 |
| 1756.63 | -7.87043 | 1756.77 | -95.9988 | 1756.71 | 73.89228 | 1756.71 | 72.0203 | 1756.71 | 24.83278 | 1756.71 | 47.98949 | 1756.71 | -28.0785 |  | 1756.71 | 45.32801 |
| 1757.26 | -7.80804 | 1757.39 | -97.0553 | 1757.34 | 74.63782 | 1757.34 | 72.33876 | 1757.34 | 25.85752 | 1757.34 | 48.47387 | 1757.34 | -25.6581 |  | 1757.34 | 46.30168 |
| 1757.88 | -7.74678 | 1758.02 | -97.7916 | 1757.96 | 75.46397 | 1757.96 | 72.55425 | 1757.96 | 27.44521 | 1757.96 | 48.85263 | 1757.96 | -22.6969 |  | 1757.96 | 47.35234 |
| 1758.51 | -7.68634 | 1758.64 | -97.9552 | 1758.59 | 76.37931 | 1758.59 | 74.07546 | 1758.59 | 28.24381 | 1758.59 | 50.53975 | 1758.59 | -20.5026 |  | 1758.59 | 48.49581 |
| 1759.13 | -7.62669 | 1759.27 | -97.658 | 1759.21 | 75.92605 | 1759.21 | 76.30566 | 1759.21 | 28.7138 | 1759.21 | 52.93322 | 1759.21 | -18.6591 |  | 1759.21 | 48.26706 |
| 1759.76 | -7.56719 | 1759.9 | -97.7903 | 1759.84 | 76.23937 | 1759.84 | 77.71303 | 1759.84 | 28.63072 | 1759.84 | 54.5065 | 1759.84 | -17.3465 |  | 1759.84 | 48.80851 |
| 1760.38 | -7.50762 | 1760.52 | -96.069 | 1760.47 | 78.17322 | 1760.47 | 79.32146 | 1760.47 | 27.71779 | 1760.47 | 56.28084 | 1760.47 | -16.8638 |  | 1760.47 | 50.97049 |
| 1761.01 | -7.44734 | 1761.15 | -97.4559 | 1761.09 | 79.22931 | 1761.09 | 80.55253 | 1761.09 | 27.17524 | 1761.09 | 57.67518 | 1761.09 | -16.0328 |  | 1761.09 | 52.25109 |
| 1761.63 | -7.38606 | 1761.77 | -96.7589 | 1761.72 | 77.93826 | 1761.72 | 79.64919 | 1761.72 | 25.74251 | 1761.72 | 56.93776 | 1761.72 | -16.0698 |  | 1761.72 | 51.18817 |
| 1762.25 | -7.32357 | 1762.4 | -96.4163 | 1762.34 | 78.14214 | 1762.34 | 79.76701 | 1762.34 | 25.0803 | 1762.34 | 57.21885 | 1762.34 | -15.3585 |  | 1762.34 | 51.61655 |
| 1762.88 | -7.25962 | 1763.02 | -95.5646 | 1762.97 | 79.40539 | 1762.97 | 78.73505 | 1762.97 | 25.62482 | 1762.97 | 56.3528 | 1762.97 | -13.4183 |  | 1762.97 | 53.10794 |
| 1763.5 | -7.19376 | 1763.65 | -96.1863 | 1763.59 | 78.99908 | 1763.59 | 79.45364 | 1763.59 | 23.22908 | 1763.59 | 57.23467 | 1763.59 | -14.4405 |  | 1763.59 | 52.92613 |
| 1764.13 | -7.12582 | 1764.27 | -95.5182 | 1764.22 | 79.11261 | 1764.22 | 79.21773 | 1764.22 | 20.72251 | 1764.22 | 57.16467 | 1764.22 | -15.5514 |  | 1764.22 | 53.2678 |
| 1764.75 | -7.05572 | 1764.9 | -94.8481 | 1764.84 | 78.74956 | 1764.84 | 79.06543 | 1764.84 | 19.36358 | 1764.84 | 57.17564 | 1764.84 | -15.5368 |  | 1764.84 | 53.12926 |
| 1765.37 | -6.98329 | 1765.52 | -93.5626 | 1765.47 | 78.89231 | 1765.47 | 79.62873 | 1765.47 | 16.80995 | 1765.47 | 57.90485 | 1765.47 | -16.6948 |  | 1765.47 | 53.50014 |
| 1766 | -6.90833 | 1766.15 | -93.515 | 1766.09 | 77.44927 | 1766.09 | 79.70349 | 1766.09 | 15.00612 | 1766.09 | 58.14289 | 1766.09 | -17.1251 |  | 1766.09 | 52.2816 |
| 1766.62 | -6.83097 | 1766.77 | -92.4208 | 1766.72 | 77.85921 | 1766.72 | 80.12472 | 1766.72 | 13.58812 | 1766.72 | 58.73003 | 1766.72 | -17.1474 |  | 1766.72 | 52.91968 |
| 1767.25 | -6.75098 | 1767.4 | -92.8175 | 1767.35 | 78.72797 | 1767.35 | 79.74085 | 1767.35 | 11.61032 | 1767.35 | 58.51207 | 1767.35 | -17.7296 |  | 1767.35 | 54.01657 |
| 1767.87 | -6.66821 | 1768.02 | -91.7072 | 1767.97 | 77.84703 | 1767.97 | 79.2904 | 1767.97 | 11.18761 | 1767.97 | 58.22489 | 1767.97 | -16.7787 |  | 1767.97 | 53.36013 |
| 1768.49 | -6.58276 | 1768.65 | -91.3066 | 1768.6 | 78.14828 | 1768.6 | 79.8323 | 1768.6 | 9.10525 | 1768.6 | 58.9327 | 1768.6 | -17.4654 |  | 1768.6 | 53.88952 |
| 1769.12 | -6.49445 | 1769.27 | -91.1115 | 1769.22 | 78.19374 | 1769.22 | 79.36624 | 1769.22 | 7.09092 | 1769.22 | 58.62992 | 1769.22 | -18.1062 |  | 1769.22 | 54.15949 |
| 1769.74 | -6.40318 | 1769.89 | -91.6146 | 1769.85 | 77.48402 | 1769.85 | 78.28402 | 1769.85 | 7.78149 | 1769.85 | 57.71361 | 1769.85 | -16.02 |  | 1769.85 | 53.6779 |
| 1770.36 | -6.30845 | 1770.52 | -90.7073 | 1770.47 | 76.57693 | 1770.47 | 78.41738 | 1770.47 | 6.72559 | 1770.47 | 58.01024 | 1770.47 | -15.7024 |  | 1770.47 | 52.99532 |
| 1770.99 | -6.21018 | 1771.14 | -90.2308 | 1771.09 | 76.72744 | 1771.09 | 78.98729 | 1771.09 | 5.19905 | 1771.09 | 58.74342 | 1771.09 | -15.8554 |  | 1771.09 | 53.37033 |
| 1771.61 | -6.10842 | 1771.77 | -90.4648 | 1771.72 | 76.74451 | 1771.72 | 80.27025 | 1771.72 | 4.33741 | 1771.72 | 60.19229 | 1771.72 | -15.3213 |  | 1771.72 | 53.61554 |
| 1772.24 | -6.00307 | 1772.39 | -90.6869 | 1772.34 | 75.66364 | 1772.34 | 79.65506 | 1772.34 | 2.08871 | 1772.34 | 59.74038 | 1772.34 | -16.1965 |  | 1772.34 | 52.75918 |
| 1772.86 | -5.89431 | 1773.02 | -91.8402 | 1772.97 | 76.45615 | 1772.97 | 78.75536 | 1772.97 | 0.24192 | 1772.97 | 59.00659 | 1772.97 | -16.6476 |  | 1772.97 | 53.77982 |
| 1773.48 | -5.78182 | 1773.64 | -92.6048 | 1773.59 | 77.98718 | 1773.59 | 79.47731 | 1773.59 | 0.34497 | 1773.59 | 59.89182 | 1773.59 | -15.6217 |  | 1773.59 | 55.53536 |
| 1774.1 | -5.66561 | 1774.27 | -92.8543 | 1774.22 | 78.06596 | 1774.22 | 79.20957 | 1774.22 | 1.63138 | 1774.22 | 59.78999 | 1774.22 | -14.4459 |  | 1774.22 | 55.84227 |
| 1774.73 | -5.54588 | 1774.89 | -92.8096 | 1774.84 | 78.53831 | 1774.84 | 79.532 | 1774.84 | 1.72069 | 1774.84 | 60.27569 | 1774.84 | -14.4655 |  | 1774.84 | 56.53912 |
| 1775.35 | -5.42288 | 1775.51 | -94.1538 | 1775.47 | 77.6567 | 1775.47 | 80.67936 | 1775.47 | 1.74259 | 1775.47 | 61.58896 | 1775.47 | -14.5543 |  | 1775.47 | 55.88564 |
| 1775.97 | -5.2966 | 1776.14 | -94.4927 | 1776.09 | 76.84786 | 1776.09 | 80.7561 | 1776.09 | 4.28483 | 1776.09 | 61.82897 | 1776.09 | -12.1209 |  | 1776.09 | 55.30132 |
| 1776.6 | -5.16741 | 1776.76 | -94.8825 | 1776.71 | 76.32015 | 1776.71 | 82.21135 | 1776.71 | 6.03507 | 1776.71 | 63.4475 | 1776.71 | -10.4796 |  | 1776.71 | 54.99811 |
| 1777.22 | -5.03564 | 1777.39 | -96.2629 | 1777.34 | 75.8143 | 1777.34 | 82.18378 | 1777.34 | 8.01803 | 1777.34 | 63.58584 | 1777.34 | -8.6073 |  | 1777.34 | 54.7204 |
| 1777.84 | -4.90148 | 1778.01 | -96.7974 | 1777.96 | 76.45717 | 1777.96 | 83.94982 | 1777.96 | 10.16415 | 1777.96 | 65.51515 | 1777.96 | -6.57009 |  | 1777.96 | 55.58778 |
| 1778.47 | -4.76489 | 1778.63 | -96.7536 | 1778.59 | 75.9974 | 1778.59 | 83.2895 | 1778.59 | 10.12477 | 1778.59 | 65.02074 | 1778.59 | -6.72014 |  | 1778.59 | 55.35614 |
| 1779.09 | -4.62592 | 1779.26 | -96.9437 | 1779.21 | 76.54806 | 1779.21 | 84.85817 | 1779.21 | 9.08749 | 1779.21 | 66.75269 | 1779.21 | -7.86632 |  | 1779.21 | 56.1313 |
| 1779.71 | -4.48471 | 1779.88 | -96.506 | 1779.83 | 76.5544 | 1779.83 | 86.67174 | 1779.83 | 8.94904 | 1779.83 | 68.72953 | 1779.83 | -8.11367 |  | 1779.83 | 56.36215 |
| 1780.33 | -4.34141 | 1780.5 | -96.6944 | 1780.46 | 78.57006 | 1780.46 | 86.5968 | 1780.46 | 10.23607 | 1780.46 | 68.8205 | 1780.46 | -6.9373 |  | 1780.46 | 58.60595 |
| 1780.96 | -4.19631 | 1781.13 | -97.8719 | 1781.08 | 78.98209 | 1781.08 | 86.86017 | 1781.08 | 13.26233 | 1781.08 | 69.24715 | 1781.08 | -4.01995 |  | 1781.08 | 59.24248 |
| 1781.58 | -4.0498 | 1781.75 | -97.46 | 1781.71 | 78.52809 | 1781.71 | 87.00394 | 1781.71 | 15.57342 | 1781.71 | 69.55683 | 1781.71 | -1.81951 |  | 1781.71 | 59.01661 |
| 1782.2 | -3.90185 | 1782.37 | -97.2197 | 1782.33 | 78.94476 | 1782.33 | 86.03818 | 1782.33 | 16.79884 | 1782.33 | 68.75435 | 1782.33 | -0.703 |  | 1782.33 | 59.65779 |
| 1782.82 | -3.75288 | 1783 | -96.6727 | 1782.95 | 79.53438 | 1782.95 | 88.09733 | 1782.95 | 18.41563 | 1782.95 | 70.97677 | 1782.95 | 0.80488 |  | 1782.95 | 60.47192 |
| 1783.45 | -3.60299 | 1783.62 | -97.0556 | 1783.58 | 79.45835 | 1783.58 | 88.61863 | 1783.58 | 19.65236 | 1783.58 | 71.66397 | 1783.58 | 1.93095 |  | 1783.58 | 60.62402 |
| 1784.07 | -3.45227 | 1784.24 | -96.7859 | 1784.2 | 80.00967 | 1784.2 | 89.47491 | 1784.2 | 20.98654 | 1784.2 | 72.68354 | 1784.2 | 3.15623 |  | 1784.2 | 61.39985 |
| 1784.69 | -3.30118 | 1784.87 | -95.4191 | 1784.82 | 80.08662 | 1784.82 | 89.27148 | 1784.82 | 20.86421 | 1784.82 | 72.64338 | 1784.82 | 2.92499 |  | 1784.82 | 61.70131 |
| 1785.31 | -3.14995 | 1785.49 | -95.0819 | 1785.45 | 80.78092 | 1785.45 | 88.23345 | 1785.45 | 21.32284 | 1785.45 | 71.77126 | 1785.45 | 3.27296 |  | 1785.45 | 62.62374 |
| 1785.94 | -2.99933 | 1786.11 | -96.1576 | 1786.07 | 80.51728 | 1786.07 | 88.35256 | 1786.07 | 21.23775 | 1786.07 | 72.05365 | 1786.07 | 3.07897 |  | 1786.07 | 62.58461 |
| 1786.56 | -2.84935 | 1786.74 | -96.6815 | 1786.69 | 81.05403 | 1786.69 | 89.7554 | 1786.69 | 22.34679 | 1786.69 | 73.61976 | 1786.69 | 4.0791 |  | 1786.69 | 63.34587 |
| 1787.18 | -2.70043 | 1787.36 | -96.9341 | 1787.32 | 82.0654 | 1787.32 | 90.12816 | 1787.32 | 26.3115 | 1787.32 | 74.15843 | 1787.32 | 7.93315 |  | 1787.32 | 64.58537 |
| 1787.8 | -2.55237 | 1787.98 | -96.0066 | 1787.94 | 82.28268 | 1787.94 | 90.57892 | 1787.94 | 27.57538 | 1787.94 | 74.77247 | 1787.94 | 9.08813 |  | 1787.94 | 65.02716 |
| 1788.42 | -2.40534 | 1788.6 | -96.0295 | 1788.56 | 82.89094 | 1788.56 | 90.91361 | 1788.56 | 31.68828 | 1788.56 | 75.27043 | 1788.56 | 13.09213 |  | 1788.56 | 65.85993 |
| 1789.04 | -2.2589 | 1789.23 | -97.2253 | 1789.19 | 82.24238 | 1789.19 | 91.16045 | 1789.19 | 33.54798 | 1789.19 | 75.68318 | 1789.19 | 14.84117 |  | 1789.19 | 65.4395 |
| 1789.67 | -2.11293 | 1789.85 | -98.8276 | 1789.81 | 83.1194 | 1789.81 | 92.62483 | 1789.81 | 34.64593 | 1789.81 | 77.31083 | 1789.81 | 15.83021 |  | 1789.81 | 66.54103 |
| 1790.29 | -1.96756 | 1790.47 | -98.7108 | 1790.43 | 84.6976 | 1790.43 | 93.76117 | 1790.43 | 35.64564 | 1790.43 | 78.61045 | 1790.43 | 16.72101 |  | 1790.43 | 68.34374 |
| 1790.91 | -1.82299 | 1791.1 | -97.5765 | 1791.06 | 85.93081 | 1791.06 | 95.03468 | 1791.06 | 36.95357 | 1791.06 | 80.04986 | 1791.06 | 17.91828 |  | 1791.06 | 69.80508 |
| 1791.53 | -1.67973 | 1791.72 | -98.0832 | 1791.68 | 86.33856 | 1791.68 | 95.05737 | 1791.68 | 38.05421 | 1791.68 | 80.23583 | 1791.68 | 18.91002 |  | 1791.68 | 70.43733 |
| 1792.15 | -1.53757 | 1792.34 | -98.8119 | 1792.3 | 87.19042 | 1792.3 | 95.82908 | 1792.3 | 41.43896 | 1792.3 | 81.17082 | 1792.3 | 22.18586 |  | 1792.3 | 71.51371 |
| 1792.77 | -1.39632 | 1792.96 | -98.8426 | 1792.92 | 87.79935 | 1792.92 | 96.15982 | 1792.92 | 44.52528 | 1792.92 | 81.66483 | 1792.92 | 25.16328 |  | 1792.92 | 72.34714 |
| 1793.4 | -1.25584 | 1793.58 | -97.8348 | 1793.55 | 88.83988 | 1793.55 | 97.79702 | 1793.55 | 48.66899 | 1793.55 | 83.46795 | 1793.55 | 29.19633 |  | 1793.55 | 73.61581 |
| 1794.02 | -1.11612 | 1794.21 | -97.755 | 1794.17 | 87.99542 | 1794.17 | 98.7396 | 1794.17 | 50.74741 | 1794.17 | 84.5738 | 1794.17 | 31.16585 |  | 1794.17 | 72.99585 |
| 1794.64 | -0.97711 | 1794.83 | -98.3488 | 1794.79 | 87.97442 | 1794.79 | 102.0433 | 1794.79 | 54.045 | 1794.79 | 88.04072 | 1794.79 | 34.35453 |  | 1794.79 | 73.19936 |
| 1795.26 | -0.83869 | 1795.45 | -98.7896 | 1795.41 | 89.29505 | 1795.41 | 104.1356 | 1795.41 | 57.45597 | 1795.41 | 90.29638 | 1795.41 | 37.6566 |  | 1795.41 | 74.7445 |
| 1795.88 | -0.70082 | 1796.07 | -97.438 | 1796.04 | 91.01696 | 1796.04 | 107.7354 | 1796.04 | 60.05144 | 1796.04 | 94.06204 | 1796.04 | 40.14141 |  | 1796.04 | 76.69454 |
| 1796.5 | -0.56348 | 1796.69 | -96.3702 | 1796.66 | 92.49851 | 1796.66 | 108.4912 | 1796.66 | 64.76922 | 1796.66 | 94.98112 | 1796.66 | 44.75029 |  | 1796.66 | 78.4006 |
| 1797.12 | -0.42681 | 1797.32 | -95.8564 | 1797.28 | 93.7528 | 1797.28 | 110.4893 | 1797.28 | 70.21014 | 1797.28 | 97.14255 | 1797.28 | 50.0823 |  | 1797.28 | 79.87941 |
| 1797.74 | -0.2907 | 1797.94 | -95.9547 | 1797.9 | 95.499 | 1797.9 | 113.0707 | 1797.9 | 75.29532 | 1797.9 | 99.8872 | 1797.9 | 55.05857 |  | 1797.9 | 81.85011 |
| 1798.36 | -0.15516 | 1798.56 | -96.1949 | 1798.53 | 97.08177 | 1798.53 | 114.1499 | 1798.53 | 79.49421 | 1798.53 | 101.1322 | 1798.53 | 59.1468 |  | 1798.53 | 83.66101 |
| 1798.99 | -0.0206 | 1799.18 | -95.5837 | 1799.15 | 98.09267 | 1799.15 | 115.073 | 1799.15 | 85.20351 | 1799.15 | 102.2187 | 1799.15 | 64.7472 |  | 1799.15 | 84.89642 |
| 1799.61 | 0.11304 | 1799.8 | -95.4446 | 1799.77 | 100.0059 | 1799.77 | 118.7297 | 1799.77 | 89.1204 | 1799.77 | 106.0387 | 1799.77 | 68.55518 |  | 1799.77 | 87.03413 |
| 1800.23 | 0.24572 | 1800.43 | -95.8806 | 1800.39 | 101.0271 | 1800.39 | 120.7428 | 1800.39 | 95.22552 | 1800.39 | 108.215 | 1800.39 | 74.5514 |  | 1800.39 | 88.27987 |
| 1800.85 | 0.37708 | 1801.05 | -95.6894 | 1801.01 | 103.4801 | 1801.01 | 123.2034 | 1801.01 | 100.8583 | 1801.01 | 110.8389 | 1801.01 | 80.07526 |  | 1801.01 | 90.95738 |
| 1801.47 | 0.5071 | 1801.67 | -95.014 | 1801.64 | 105.7318 | 1801.64 | 125.2349 | 1801.64 | 104.2765 | 1801.64 | 113.0363 | 1801.64 | 83.3828 |  | 1801.64 | 93.43718 |
| 1802.09 | 0.63595 | 1802.29 | -94.7178 | 1802.26 | 108.0049 | 1802.26 | 126.5445 | 1802.26 | 108.5045 | 1802.26 | 114.5092 | 1802.26 | 87.5019 |  | 1802.26 | 95.93483 |
| 1802.71 | 0.76367 | 1802.91 | -95.0559 | 1802.88 | 110.0186 | 1802.88 | 128.3842 | 1802.88 | 112.5713 | 1802.88 | 116.5122 | 1802.88 | 91.45983 |  | 1802.88 | 98.17306 |
| 1803.33 | 0.89025 | 1803.53 | -95.1408 | 1803.5 | 113.1298 | 1803.5 | 130.71 | 1803.5 | 115.8395 | 1803.5 | 119.0012 | 1803.5 | 94.61908 |  | 1803.5 | 101.5087 |
| 1803.95 | 1.01557 | 1804.15 | -95.8349 | 1804.12 | 114.6338 | 1804.12 | 133.2712 | 1804.12 | 122.5327 | 1804.12 | 121.7257 | 1804.12 | 101.2034 |  | 1804.12 | 103.2373 |
| 1804.57 | 1.13972 | 1804.78 | -96.1397 | 1804.74 | 116.2914 | 1804.74 | 136.9236 | 1804.74 | 129.1668 | 1804.74 | 125.5414 | 1804.74 | 107.7286 |  | 1804.74 | 105.1194 |
| 1805.19 | 1.26235 | 1805.4 | -96.2324 | 1805.36 | 117.5917 | 1805.36 | 139.1896 | 1805.36 | 133.2204 | 1805.36 | 127.9707 | 1805.36 | 111.6732 |  | 1805.36 | 106.6441 |
| 1805.81 | 1.38356 | 1806.02 | -97.6356 | 1805.99 | 120.5301 | 1805.99 | 140.2785 | 1805.99 | 135.9775 | 1805.99 | 129.2255 | 1805.99 | 114.3197 |  | 1805.99 | 109.8107 |
| 1806.43 | 1.50327 | 1806.64 | -97.1632 | 1806.61 | 123.008 | 1806.61 | 142.819 | 1806.61 | 139.641 | 1806.61 | 131.9293 | 1806.61 | 117.8744 |  | 1806.61 | 112.5131 |
| 1807.05 | 1.62127 | 1807.26 | -97.6287 | 1807.23 | 125.2704 | 1807.23 | 145.1604 | 1807.23 | 144.0003 | 1807.23 | 134.434 | 1807.23 | 122.1247 |  | 1807.23 | 115 |
| 1807.67 | 1.73734 | 1807.88 | -98.0155 | 1807.85 | 127.9804 | 1807.85 | 146.6152 | 1807.85 | 146.9499 | 1807.85 | 136.052 | 1807.85 | 124.9654 |  | 1807.85 | 117.9345 |
| 1808.29 | 1.85137 | 1808.5 | -97.9213 | 1808.47 | 129.5751 | 1808.47 | 148.6132 | 1808.47 | 150.2767 | 1808.47 | 138.2133 | 1808.47 | 128.1833 |  | 1808.47 | 119.7537 |
| 1808.91 | 1.9632 | 1809.12 | -99.1706 | 1809.09 | 130.9722 | 1809.09 | 152.1154 | 1809.09 | 151.2342 | 1809.09 | 141.8787 | 1809.09 | 129.0319 |  | 1809.09 | 121.3753 |
| 1809.53 | 2.07257 | 1809.74 | -99.6332 | 1809.71 | 130.9429 | 1809.71 | 151.9622 | 1809.71 | 153.8071 | 1809.71 | 141.8888 | 1809.71 | 131.4959 |  | 1809.71 | 121.5706 |
| 1810.15 | 2.17924 | 1810.36 | -99.9926 | 1810.33 | 130.7448 | 1810.33 | 153.8995 | 1810.33 | 157.0757 | 1810.33 | 143.9894 | 1810.33 | 134.6556 |  | 1810.33 | 121.597 |
| 1810.77 | 2.28329 | 1810.98 | -99.9109 | 1810.96 | 132.0227 | 1810.96 | 154.4727 | 1810.96 | 160.2354 | 1810.96 | 144.7285 | 1810.96 | 137.7046 |  | 1810.96 | 123.103 |
| 1811.39 | 2.38465 | 1811.61 | -100.802 | 1811.58 | 133.9601 | 1811.58 | 154.4034 | 1811.58 | 162.6465 | 1811.58 | 144.8225 | 1811.58 | 140.0069 |  | 1811.58 | 125.2649 |
| 1812.01 | 2.48368 | 1812.23 | -101.445 | 1812.2 | 135.371 | 1812.2 | 155.83 | 1812.2 | 164.5705 | 1812.2 | 146.4124 | 1812.2 | 141.822 |  | 1812.2 | 126.9003 |
| 1812.63 | 2.58052 | 1812.85 | -99.6474 | 1812.82 | 136.8397 | 1812.82 | 157.2251 | 1812.82 | 166.7185 | 1812.82 | 147.9708 | 1812.82 | 143.861 |  | 1812.82 | 128.5936 |
| 1813.25 | 2.67481 | 1813.47 | -99.3049 | 1813.44 | 138.0934 | 1813.44 | 158.282 | 1813.44 | 168.3803 | 1813.44 | 149.1909 | 1813.44 | 145.4139 |  | 1813.44 | 130.0717 |
| 1813.87 | 2.76636 | 1814.09 | -99.3305 | 1814.06 | 138.6603 | 1814.06 | 160.2633 | 1814.06 | 170.1643 | 1814.06 | 151.3355 | 1814.06 | 147.0891 |  | 1814.06 | 130.8632 |
| 1814.49 | 2.85543 | 1814.71 | -98.7176 | 1814.68 | 139.1776 | 1814.68 | 158.9918 | 1814.68 | 172.9557 | 1814.68 | 150.2273 | 1814.68 | 149.7716 |  | 1814.68 | 131.605 |
| 1815.11 | 2.94185 | 1815.33 | -98.2413 | 1815.3 | 139.528 | 1815.3 | 160.4987 | 1815.3 | 175.9165 | 1815.3 | 151.8974 | 1815.3 | 152.6234 |  | 1815.3 | 132.1798 |
| 1815.73 | 3.02573 | 1815.95 | -97.2811 | 1815.92 | 140.4262 | 1815.92 | 162.2694 | 1815.92 | 178.462 | 1815.92 | 153.8314 | 1815.92 | 155.06 |  | 1815.92 | 133.3025 |
| 1816.35 | 3.10742 | 1816.57 | -97.3437 | 1816.54 | 142.0805 | 1816.54 | 162.8204 | 1816.54 | 181.4092 | 1816.54 | 154.5456 | 1816.54 | 157.8983 |  | 1816.54 | 135.1813 |
| 1816.96 | 3.18678 | 1817.19 | -97.0391 | 1817.16 | 143.1087 | 1817.16 | 165.0127 | 1817.16 | 183.8835 | 1817.16 | 156.9012 | 1817.16 | 160.2637 |  | 1817.16 | 136.4341 |
| 1817.58 | 3.26394 | 1817.81 | -96.5069 | 1817.78 | 143.5676 | 1817.78 | 166.467 | 1817.78 | 186.1909 | 1817.78 | 158.5189 | 1817.78 | 162.4622 |  | 1817.78 | 137.1175 |
| 1818.2 | 3.33855 | 1818.43 | -96.0382 | 1818.4 | 144.4846 | 1818.4 | 166.5722 | 1818.4 | 189.2567 | 1818.4 | 158.7873 | 1818.4 | 165.4191 |  | 1818.4 | 138.259 |
| 1818.82 | 3.41068 | 1819.05 | -95.1406 | 1819.02 | 144.8888 | 1819.02 | 166.7218 | 1819.02 | 189.8766 | 1819.02 | 159.1002 | 1819.02 | 165.9301 |  | 1819.02 | 138.8877 |
| 1819.44 | 3.48033 | 1819.67 | -96.7451 | 1819.64 | 146.2487 | 1819.64 | 167.4401 | 1819.64 | 191.6875 | 1819.64 | 159.9818 | 1819.64 | 167.6321 |  | 1819.64 | 140.4721 |
| 1820.06 | 3.54781 | 1820.29 | -97.3505 | 1820.26 | 147.2196 | 1820.26 | 167.4693 | 1820.26 | 192.7926 | 1820.26 | 160.1743 | 1820.26 | 168.6282 |  | 1820.26 | 141.6675 |
| 1820.68 | 3.61342 | 1820.91 | -96.4666 | 1820.88 | 148.9628 | 1820.88 | 167.8589 | 1820.88 | 196.0462 | 1820.88 | 160.7271 | 1820.88 | 171.7729 |  | 1820.88 | 143.6352 |
| 1821.3 | 3.67745 | 1821.53 | -96.65 | 1821.5 | 150.1544 | 1821.5 | 168.6739 | 1821.5 | 197.379 | 1821.5 | 161.7054 | 1821.5 | 172.9968 |  | 1821.5 | 145.0514 |
| 1821.92 | 3.74026 | 1822.15 | -96.7289 | 1822.12 | 149.536 | 1822.12 | 168.4418 | 1822.12 | 199.5664 | 1822.12 | 161.6365 | 1822.12 | 175.0754 |  | 1822.12 | 144.6574 |
| 1822.53 | 3.80208 | 1822.76 | -96.9437 | 1822.74 | 149.2981 | 1822.74 | 168.8563 | 1822.74 | 201.9455 | 1822.74 | 162.2143 | 1822.74 | 177.3455 |  | 1822.74 | 144.6441 |
| 1823.15 | 3.86283 | 1823.39 | -96.4887 | 1823.36 | 149.7371 | 1823.36 | 170.3604 | 1823.36 | 204.5037 | 1823.36 | 163.8817 | 1823.36 | 179.7949 |  | 1823.36 | 145.3076 |
| 1823.77 | 3.92231 | 1824 | -97.2756 | 1823.98 | 149.7416 | 1823.98 | 171.4167 | 1823.98 | 205.5563 | 1823.98 | 165.1013 | 1823.98 | 180.7385 |  | 1823.98 | 145.5366 |
| 1824.39 | 3.9808 | 1824.62 | -96.4464 | 1824.6 | 151.2166 | 1824.6 | 171.5419 | 1824.6 | 206.4731 | 1824.6 | 165.3898 | 1824.6 | 181.5464 |  | 1824.6 | 147.2361 |
| 1825.01 | 4.0383 | 1825.24 | -96.4453 | 1825.22 | 150.2791 | 1825.22 | 171.3777 | 1825.22 | 208.3703 | 1825.22 | 165.3888 | 1825.22 | 183.3347 |  | 1825.22 | 146.5231 |
| 1825.63 | 4.09504 | 1825.86 | -97.1019 | 1825.84 | 152.1524 | 1825.84 | 170.9601 | 1825.84 | 210.1332 | 1825.84 | 165.1345 | 1825.84 | 184.9887 |  | 1825.84 | 148.6209 |
| 1826.24 | 4.15119 | 1826.48 | -96.665 | 1826.46 | 153.8066 | 1826.46 | 170.6114 | 1826.46 | 210.3322 | 1826.46 | 164.9491 | 1826.46 | 185.0788 |  | 1826.46 | 150.4997 |
| 1826.86 | 4.20679 | 1827.1 | -95.9987 | 1827.08 | 154.8043 | 1827.08 | 170.3296 | 1827.08 | 212.2688 | 1827.08 | 164.8306 | 1827.08 | 186.9065 |  | 1827.08 | 151.7219 |
| 1827.48 | 4.26202 | 1827.72 | -96.6592 | 1827.7 | 155.6791 | 1827.7 | 168.7963 | 1827.7 | 214.9794 | 1827.7 | 163.4606 | 1827.7 | 189.5082 |  | 1827.7 | 152.8211 |
| 1828.1 | 4.31682 | 1828.34 | -97.4304 | 1828.32 | 157.0046 | 1828.32 | 169.0742 | 1828.32 | 215.4977 | 1828.32 | 163.9018 | 1828.32 | 189.9176 |  | 1828.32 | 154.3711 |
| 1828.72 | 4.37133 | 1828.96 | -98.8054 | 1828.94 | 157.3195 | 1828.94 | 169.92 | 1828.94 | 214.3828 | 1828.94 | 164.9108 | 1828.94 | 188.6938 |  | 1828.94 | 154.9105 |
| 1829.33 | 4.42553 | 1829.58 | -98.4084 | 1829.56 | 157.0734 | 1829.56 | 171.2604 | 1829.56 | 215.2976 | 1829.56 | 166.4145 | 1829.56 | 189.4997 |  | 1829.56 | 154.889 |
| 1829.95 | 4.47963 | 1830.19 | -96.8502 | 1830.18 | 157.3459 | 1830.18 | 172.1341 | 1830.18 | 216.5527 | 1830.18 | 167.4515 | 1830.18 | 190.6459 |  | 1830.18 | 155.386 |
| 1830.57 | 4.53353 | 1830.81 | -95.8739 | 1830.79 | 157.1744 | 1830.79 | 171.8549 | 1830.79 | 215.9327 | 1830.79 | 167.3329 | 1830.79 | 189.9187 |  | 1830.79 | 155.4353 |
| 1831.19 | 4.58697 | 1831.43 | -96.9944 | 1831.41 | 157.5618 | 1831.41 | 171.3515 | 1831.41 | 215.9983 | 1831.41 | 166.9928 | 1831.41 | 189.8755 |  | 1831.41 | 156.0472 |
| 1831.81 | 4.63977 | 1832.05 | -95.9823 | 1832.03 | 158.3946 | 1832.03 | 170.8464 | 1832.03 | 215.3332 | 1832.03 | 166.6509 | 1832.03 | 189.1015 |  | 1832.03 | 157.1046 |
| 1832.42 | 4.69173 | 1832.67 | -95.735 | 1832.65 | 157.3239 | 1832.65 | 170.2331 | 1832.65 | 215.3632 | 1832.65 | 166.2009 | 1832.65 | 189.0225 |  | 1832.65 | 156.2584 |
| 1833.04 | 4.74272 | 1833.29 | -94.9311 | 1833.27 | 157.7125 | 1833.27 | 169.4341 | 1833.27 | 216.0682 | 1833.27 | 165.5652 | 1833.27 | 189.6186 |  | 1833.27 | 156.8715 |
| 1833.66 | 4.79265 | 1833.91 | -95.1197 | 1833.89 | 156.8084 | 1833.89 | 171.2159 | 1833.89 | 217.1799 | 1833.89 | 167.5103 | 1833.89 | 190.6214 |  | 1833.89 | 156.1919 |
| 1834.28 | 4.84191 | 1834.52 | -95.1775 | 1834.51 | 155.9607 | 1834.51 | 170.0432 | 1834.51 | 217.2351 | 1834.51 | 166.5008 | 1834.51 | 190.5678 |  | 1834.51 | 155.5687 |
| 1834.89 | 4.89101 | 1835.14 | -94.4574 | 1835.13 | 155.0987 | 1835.13 | 169.898 | 1835.13 | 216.1027 | 1835.13 | 166.5189 | 1835.13 | 189.3264 |  | 1835.13 | 154.9313 |
| 1835.51 | 4.94055 | 1835.76 | -92.7884 | 1835.75 | 153.836 | 1835.75 | 169.4283 | 1835.75 | 214.7478 | 1835.75 | 166.2125 | 1835.75 | 187.8627 |  | 1835.75 | 153.893 |
| 1836.13 | 4.99075 | 1836.38 | -93.2358 | 1836.36 | 153.1859 | 1836.36 | 168.004 | 1836.36 | 213.7344 | 1836.36 | 164.9488 | 1836.36 | 186.7421 |  | 1836.36 | 153.4639 |
| 1836.75 | 5.03964 | 1837 | -94.5449 | 1836.98 | 152.4275 | 1836.98 | 167.0868 | 1836.98 | 214.9703 | 1836.98 | 164.1949 | 1836.98 | 187.8691 |  | 1836.98 | 152.9299 |
| 1837.36 | 5.08612 | 1837.62 | -95.1126 | 1837.6 | 151.3806 | 1837.6 | 167.4617 | 1837.6 | 215.0225 | 1837.6 | 164.733 | 1837.6 | 187.8123 |  | 1837.6 | 152.1075 |
| 1837.98 | 5.13026 | 1838.23 | -94.7797 | 1838.22 | 150.3488 | 1838.22 | 166.6922 | 1838.22 | 215.9715 | 1838.22 | 164.1269 | 1838.22 | 188.6525 |  | 1838.22 | 151.3002 |
| 1838.6 | 5.17404 | 1838.85 | -94.7383 | 1838.84 | 150.095 | 1838.84 | 165.9981 | 1838.84 | 216.0572 | 1838.84 | 163.5961 | 1838.84 | 188.6293 |  | 1838.84 | 151.271 |
| 1839.21 | 5.21577 | 1839.47 | -95.0121 | 1839.46 | 149.3184 | 1839.46 | 167.1443 | 1839.46 | 215.6509 | 1839.46 | 164.9055 | 1839.46 | 188.1141 |  | 1839.46 | 150.7189 |
| 1839.83 | 5.25538 | 1840.09 | -96.4065 | 1840.07 | 149.7243 | 1840.07 | 166.556 | 1840.07 | 217.2438 | 1840.07 | 164.4779 | 1840.07 | 189.5998 |  | 1840.07 | 151.3457 |
| 1840.45 | 5.29361 | 1840.71 | -96.9582 | 1840.69 | 150.5915 | 1840.69 | 165.4055 | 1840.69 | 220.1193 | 1840.69 | 163.4907 | 1840.69 | 192.3664 |  | 1840.69 | 152.4373 |
| 1841.06 | 5.33157 | 1841.32 | -96.5452 | 1841.31 | 151.868 | 1841.31 | 165.4394 | 1841.31 | 220.6867 | 1841.31 | 163.6878 | 1841.31 | 192.8249 |  | 1841.31 | 153.9384 |
| 1841.68 | 5.36613 | 1841.94 | -95.936 | 1841.93 | 153.0766 | 1841.93 | 165.3676 | 1841.93 | 221.8707 | 1841.93 | 163.7793 | 1841.93 | 193.9 |  | 1841.93 | 155.3715 |
| 1842.3 | 5.39124 | 1842.56 | -96.8851 | 1842.55 | 153.4809 | 1842.55 | 166.1139 | 1842.55 | 222.8176 | 1842.55 | 164.6889 | 1842.55 | 194.738 |  | 1842.55 | 156.0003 |
| 1842.91 | 5.40621 | 1843.18 | -96.8256 | 1843.16 | 153.5832 | 1843.16 | 166.0445 | 1843.16 | 224.4083 | 1843.16 | 164.7801 | 1843.16 | 196.2215 |  | 1843.16 | 156.3234 |
| 1843.53 | 5.41173 | 1843.79 | -96.8311 | 1843.78 | 153.1363 | 1843.78 | 166.8126 | 1843.78 | 226.7274 | 1843.78 | 165.7114 | 1843.78 | 198.4317 |  | 1843.78 | 156.1011 |
| 1844.15 | 5.41378 | 1844.41 | -96.6838 | 1844.4 | 153.0491 | 1844.4 | 166.7725 | 1844.4 | 228.3093 | 1844.4 | 165.8347 | 1844.4 | 199.9047 |  | 1844.4 | 156.2384 |
| 1844.76 | 5.41262 | 1845.03 | -96.7571 | 1845.02 | 153.19 | 1845.02 | 167.0393 | 1845.02 | 229.2393 | 1845.02 | 166.2647 | 1845.02 | 200.7258 |  | 1845.02 | 156.6039 |
| 1845.38 | 5.40566 | 1845.65 | -97.9994 | 1845.63 | 152.4281 | 1845.63 | 166.5632 | 1845.63 | 229.6401 | 1845.63 | 165.9493 | 1845.63 | 201.0195 |  | 1845.63 | 156.0628 |
| 1846 | 5.39457 | 1846.26 | -97.5927 | 1846.25 | 152.1799 | 1846.25 | 167.5033 | 1846.25 | 230.3757 | 1846.25 | 167.0526 | 1846.25 | 201.6462 |  | 1846.25 | 156.0391 |
| 1846.61 | 5.37301 | 1846.88 | -96.4553 | 1846.87 | 152.3077 | 1846.87 | 167.6585 | 1846.87 | 230.965 | 1846.87 | 167.3711 | 1846.87 | 202.1265 |  | 1846.87 | 156.3914 |
| 1847.23 | 5.3263 | 1847.5 | -96.433 | 1847.49 | 152.4666 | 1847.49 | 167.3471 | 1847.49 | 231.1612 | 1847.49 | 167.223 | 1847.49 | 202.2138 |  | 1847.49 | 156.7748 |
| 1847.84 | 5.24206 | 1848.11 | -96.6355 | 1848.1 | 151.2357 | 1848.1 | 168.3669 | 1848.1 | 232.7759 | 1848.1 | 168.4034 | 1848.1 | 203.7214 |  | 1848.1 | 155.7648 |
| 1848.46 | 5.24921 | 1848.73 | -97.2465 | 1848.72 | 150.4062 | 1848.72 | 167.6026 | 1848.72 | 233.025 | 1848.72 | 167.8024 | 1848.72 | 203.8616 |  | 1848.72 | 155.1598 |
| 1849.08 | 5.25763 | 1849.35 | -96.9137 | 1849.34 | 151.8142 | 1849.34 | 168.3617 | 1849.34 | 233.4963 | 1849.34 | 168.7248 | 1849.34 | 204.224 |  | 1849.34 | 156.7924 |
| 1849.69 | 5.26649 | 1849.97 | -96.4467 | 1849.96 | 152.3364 | 1849.96 | 168.021 | 1849.96 | 232.8072 | 1849.96 | 168.5474 | 1849.96 | 203.426 |  | 1849.96 | 157.539 |
| 1850.31 | 5.27648 | 1850.58 | -96.3716 | 1850.57 | 152.8293 | 1850.57 | 168.7232 | 1850.57 | 233.9813 | 1850.57 | 169.4103 | 1850.57 | 204.493 |  | 1850.57 | 158.2529 |
| 1850.92 | 5.28908 | 1851.2 | -96.4162 | 1851.19 | 152.4393 | 1851.19 | 168.5589 | 1851.19 | 235.4759 | 1851.19 | 169.4092 | 1851.19 | 205.8786 |  | 1851.19 | 158.0873 |
| 1851.54 | 5.30449 | 1851.82 | -96.2843 | 1851.81 | 152.4891 | 1851.81 | 169.071 | 1851.81 | 235.1407 | 1851.81 | 170.0845 | 1851.81 | 205.4346 |  | 1851.81 | 158.3617 |
| 1852.16 | 5.32333 | 1852.43 | -95.5052 | 1852.42 | 151.5406 | 1852.42 | 169.4769 | 1852.42 | 235.8802 | 1852.42 | 170.6511 | 1852.42 | 206.0669 |  | 1852.42 | 157.634 |
| 1852.77 | 5.3462 | 1853.05 | -95.4896 | 1853.04 | 151.0085 | 1853.04 | 167.7662 | 1853.04 | 237.6315 | 1853.04 | 169.1037 | 1853.04 | 207.7093 |  | 1853.04 | 157.3264 |
| 1853.39 | 5.3737 | 1853.67 | -94.8 | 1853.66 | 151.1595 | 1853.66 | 167.1482 | 1853.66 | 238.3835 | 1853.66 | 168.649 | 1853.66 | 208.3524 |  | 1853.66 | 157.702 |
| 1854 | 5.4072 | 1854.28 | -93.4835 | 1854.28 | 151.6241 | 1854.28 | 167.005 | 1854.28 | 238.2015 | 1854.28 | 168.669 | 1854.28 | 208.0615 |  | 1854.28 | 158.3911 |
| 1854.62 | 5.44789 | 1854.9 | -92.8421 | 1854.89 | 151.3042 | 1854.89 | 166.6821 | 1854.89 | 235.8758 | 1854.89 | 168.5067 | 1854.89 | 205.6286 |  | 1854.89 | 158.2921 |
| 1855.23 | 5.49696 | 1855.51 | -92.2039 | 1855.51 | 151.4948 | 1855.51 | 165.3122 | 1855.51 | 235.9923 | 1855.51 | 167.3002 | 1855.51 | 205.6363 |  | 1855.51 | 158.7072 |
| 1855.85 | 5.55417 | 1856.13 | -92.7864 | 1856.13 | 150.8146 | 1856.13 | 165.4614 | 1856.13 | 236.8087 | 1856.13 | 167.6126 | 1856.13 | 206.3438 |  | 1856.13 | 158.2515 |
| 1856.46 | 5.62007 | 1856.75 | -93.2946 | 1856.74 | 152.0743 | 1856.74 | 165.266 | 1856.74 | 236.141 | 1856.74 | 167.5778 | 1856.74 | 205.5689 |  | 1856.74 | 159.7321 |
| 1857.08 | 5.69441 | 1857.36 | -93.019 | 1857.36 | 151.9688 | 1857.36 | 165.8403 | 1857.36 | 237.6315 | 1857.36 | 168.3155 | 1857.36 | 206.9505 |  | 1857.36 | 159.8511 |
| 1857.7 | 5.7785 | 1857.98 | -93.0706 | 1857.97 | 150.6024 | 1857.97 | 166.1987 | 1857.97 | 238.1267 | 1857.97 | 168.8345 | 1857.97 | 207.3385 |  | 1857.97 | 158.7056 |
| 1858.31 | 5.87386 | 1858.6 | -92.7021 | 1858.59 | 149.4211 | 1858.59 | 165.7762 | 1858.59 | 238.7504 | 1858.59 | 168.5753 | 1858.59 | 207.8533 |  | 1858.59 | 157.7488 |
| 1858.93 | 5.98129 | 1859.21 | -92.809 | 1859.21 | 147.7258 | 1859.21 | 166.2241 | 1859.21 | 238.0652 | 1859.21 | 169.1865 | 1859.21 | 207.0592 |  | 1859.21 | 156.2779 |
| 1859.54 | 6.10137 | 1859.83 | -92.3489 | 1859.82 | 147.0707 | 1859.82 | 166.1883 | 1859.82 | 236.3405 | 1859.82 | 169.3112 | 1859.82 | 205.2274 |  | 1859.82 | 155.8437 |
| 1860.16 | 6.23469 | 1860.44 | -93.3176 | 1860.44 | 147.0443 | 1860.44 | 164.8113 | 1860.44 | 237.743 | 1860.44 | 168.0976 | 1860.44 | 206.521 |  | 1860.44 | 156.0419 |
| 1860.17 | 6.3824 | 1861.06 | -93.8798 | 1861.06 | 147.4545 | 1861.06 | 162.5949 | 1861.06 | 236.4552 | 1861.06 | 166.0444 | 1861.06 | 205.1242 |  | 1861.06 | 156.6766 |
| 1860.78 | 6.54502 | 1861.68 | -94.4579 | 1861.67 | 147.2848 | 1861.67 | 162.2444 | 1861.67 | 235.0812 | 1861.67 | 165.8545 | 1861.67 | 203.6431 |  | 1861.67 | 156.7278 |
| 1861.4 | 6.72211 | 1862.29 | -94.6828 | 1862.29 | 146.3662 | 1862.29 | 162.4656 | 1862.29 | 235.0184 | 1862.29 | 166.239 | 1862.29 | 203.4714 |  | 1862.29 | 156.0337 |
| 1862.02 | 6.91447 | 1862.91 | -93.9276 | 1862.9 | 145.1367 | 1862.9 | 160.6924 | 1862.9 | 234.6034 | 1862.9 | 164.6265 | 1862.9 | 202.9493 |  | 1862.9 | 155.0251 |
| 1862.63 | 7.12307 | 1863.52 | -94.332 | 1863.52 | 143.7078 | 1863.52 | 159.8476 | 1863.52 | 233.4055 | 1863.52 | 163.945 | 1863.52 | 201.6424 |  | 1863.52 | 153.8207 |
| 1863.25 | 7.34808 | 1864.14 | -94.2799 | 1864.14 | 143.4096 | 1864.14 | 159.3081 | 1864.14 | 231.1301 | 1864.14 | 163.5687 | 1864.14 | 199.2582 |  | 1864.14 | 153.747 |
| 1863.87 | 7.59019 | 1864.75 | -95.1385 | 1864.75 | 143.0732 | 1864.75 | 159.8318 | 1864.75 | 228.3443 | 1864.75 | 164.2531 | 1864.75 | 196.3652 |  | 1864.75 | 153.6314 |
| 1864.48 | 7.84947 | 1865.37 | -95.0886 | 1865.37 | 142.0031 | 1865.37 | 157.7523 | 1865.37 | 226.6875 | 1865.37 | 162.3369 | 1865.37 | 194.5995 |  | 1865.37 | 152.7859 |
| 1865.1 | 8.12629 | 1865.98 | -94.6893 | 1865.98 | 141.4717 | 1865.98 | 156.1712 | 1865.98 | 224.4411 | 1865.98 | 160.9164 | 1865.98 | 192.2459 |  | 1865.98 | 152.4754 |
| 1865.72 | 8.42116 | 1866.6 | -94.8863 | 1866.6 | 140.7494 | 1866.6 | 154.6622 | 1866.6 | 223.2407 | 1866.6 | 159.5707 | 1866.6 | 190.9367 |  | 1866.6 | 151.9776 |
| 1866.33 | 8.73432 | 1867.21 | -94.5825 | 1867.21 | 140.7659 | 1867.21 | 152.3155 | 1867.21 | 221.9639 | 1867.21 | 157.3846 | 1867.21 | 189.5527 |  | 1867.21 | 152.2149 |
| 1866.95 | 9.06475 | 1867.83 | -94.4127 | 1867.83 | 140.6124 | 1867.83 | 151.0385 | 1867.83 | 221.1137 | 1867.83 | 156.2709 | 1867.83 | 188.5936 |  | 1867.83 | 152.286 |
| 1867.56 | 9.41178 | 1868.44 | -93.8709 | 1868.44 | 139.8386 | 1868.44 | 150.7563 | 1868.44 | 219.5492 | 1868.44 | 156.1493 | 1868.44 | 186.9219 |  | 1868.44 | 151.7331 |
| 1868.18 | 9.7739 | 1869.06 | -94.3498 | 1869.06 | 138.6467 | 1869.06 | 149.6659 | 1869.06 | 219.175 | 1869.06 | 155.2223 | 1869.06 | 186.4389 |  | 1869.06 | 150.7657 |
| 1868.8 | 10.15038 | 1869.67 | -94.8471 | 1869.68 | 137.3665 | 1869.68 | 148.5714 | 1869.68 | 215.8862 | 1869.68 | 154.291 | 1869.68 | 183.0411 |  | 1869.68 | 149.71 |
| 1869.41 | 10.54181 | 1870.29 | -94.2659 | 1870.29 | 135.961 | 1870.29 | 146.946 | 1870.29 | 213.0078 | 1870.29 | 152.8262 | 1870.29 | 180.0556 |  | 1870.29 | 148.5254 |
| 1870.03 | 10.94869 | 1870.9 | -94.6483 | 1870.91 | 133.981 | 1870.91 | 145.5814 | 1870.91 | 212.2872 | 1870.91 | 151.625 | 1870.91 | 179.226 |  | 1870.91 | 146.7699 |
| 1870.64 | 11.37054 | 1871.52 | -94.3146 | 1871.52 | 132.3218 | 1871.52 | 144.6696 | 1871.52 | 208.4086 | 1871.52 | 150.8737 | 1871.52 | 175.2403 |  | 1871.52 | 145.3316 |
| 1871.26 | 11.80505 | 1872.14 | -94.8549 | 1872.14 | 130.7082 | 1872.14 | 142.5788 | 1872.14 | 206.2891 | 1872.14 | 148.9463 | 1872.14 | 173.0119 |  | 1872.14 | 143.9425 |
| 1871.87 | 12.25063 | 1872.75 | -95.0528 | 1872.75 | 129.321 | 1872.75 | 141.7243 | 1872.75 | 204.5768 | 1872.75 | 148.2523 | 1872.75 | 171.1925 |  | 1872.75 | 142.7761 |
| 1872.49 | 12.70568 | 1873.36 | -95.0501 | 1873.37 | 128.1167 | 1873.37 | 140.3628 | 1873.37 | 200.7319 | 1873.37 | 147.0541 | 1873.37 | 167.2387 |  | 1873.37 | 141.7964 |
| 1873.11 | 13.16981 | 1873.98 | -94.9575 | 1873.98 | 125.8161 | 1873.98 | 139.2661 | 1873.98 | 197.4989 | 1873.98 | 146.118 | 1873.98 | 163.8985 |  | 1873.98 | 139.7167 |
| 1873.72 | 13.64233 | 1874.59 | -95.6365 | 1874.6 | 123.4819 | 1874.6 | 138.2956 | 1874.6 | 194.9801 | 1874.6 | 145.3108 | 1874.6 | 161.2708 |  | 1874.6 | 137.607 |
| 1874.34 | 14.1228 | 1875.21 | -96.7888 | 1875.21 | 121.3842 | 1875.21 | 136.7312 | 1875.21 | 190.2354 | 1875.21 | 143.9071 | 1875.21 | 156.4189 |  | 1875.21 | 135.7301 |
| 1874.95 | 14.61065 | 1875.82 | -96.3712 | 1875.83 | 119.4825 | 1875.83 | 134.3917 | 1875.83 | 184.8466 | 1875.83 | 141.7308 | 1875.83 | 150.9212 |  | 1875.83 | 134.0529 |
| 1875.57 | 15.10523 | 1876.44 | -96.6885 | 1876.44 | 117.7112 | 1876.44 | 131.9639 | 1876.44 | 181.7001 | 1876.44 | 139.4637 | 1876.44 | 147.6676 |  | 1876.44 | 132.5025 |
| 1876.18 | 15.60555 | 1877.05 | -96.3476 | 1877.05 | 116.5036 | 1877.05 | 130.0476 | 1877.05 | 180.1245 | 1877.05 | 137.7081 | 1877.05 | 145.9849 |  | 1877.05 | 131.5158 |
| 1876.8 | 16.11206 | 1877.67 | -96.084 | 1877.67 | 115.5208 | 1877.67 | 127.6266 | 1877.67 | 176.7623 | 1877.67 | 135.4503 | 1877.67 | 142.5138 |  | 1877.67 | 130.7576 |
| 1877.41 | 16.62397 | 1878.28 | -95.416 | 1878.28 | 114.0303 | 1878.28 | 125.4468 | 1878.28 | 174.035 | 1878.28 | 133.4312 | 1878.28 | 139.6793 |  | 1878.28 | 129.4879 |
| 1878.03 | 17.13952 | 1878.89 | -95.3489 | 1878.9 | 111.1667 | 1878.9 | 123.7184 | 1878.9 | 172.5402 | 1878.9 | 131.8661 | 1878.9 | 138.0756 |  | 1878.9 | 126.8489 |
| 1878.64 | 17.65977 | 1879.51 | -96.6118 | 1879.51 | 110.1745 | 1879.51 | 120.8369 | 1879.51 | 169.4067 | 1879.51 | 129.1452 | 1879.51 | 134.835 |  | 1879.51 | 126.0776 |
| 1879.26 | 18.18431 | 1880.12 | -97.3365 | 1880.13 | 108.5569 | 1880.13 | 118.7816 | 1880.13 | 166.9629 | 1880.13 | 127.2532 | 1880.13 | 132.2822 |  | 1880.13 | 124.6845 |
| 1879.87 | 18.71232 | 1880.74 | -98.1739 | 1880.74 | 105.6242 | 1880.74 | 116.444 | 1880.74 | 163.8429 | 1880.74 | 125.0762 | 1880.74 | 129.0551 |  | 1880.74 | 121.9726 |
| 1880.49 | 19.24339 | 1881.35 | -97.5977 | 1881.36 | 102.8699 | 1881.36 | 115.1964 | 1881.36 | 160.1976 | 1881.36 | 123.9919 | 1881.36 | 125.3009 |  | 1881.36 | 119.4428 |
| 1881.1 | 19.77914 | 1881.96 | -96.0753 | 1881.97 | 99.22064 | 1881.97 | 111.6967 | 1881.97 | 154.9293 | 1881.97 | 120.6528 | 1881.97 | 119.9254 |  | 1881.97 | 116.0145 |
| 1881.72 | 20.32074 | 1882.58 | -96.6563 | 1882.58 | 95.91683 | 1882.58 | 108.7984 | 1882.58 | 149.2173 | 1882.58 | 117.9151 | 1882.58 | 114.1063 |  | 1882.58 | 112.9316 |
| 1882.33 | 20.86897 | 1883.19 | -95.5979 | 1883.2 | 93.19607 | 1883.2 | 106.1774 | 1883.2 | 146.3789 | 1883.2 | 115.4575 | 1883.2 | 111.159 |  | 1883.2 | 110.4353 |
| 1882.95 | 21.4221 | 1883.81 | -96.376 | 1883.81 | 91.40103 | 1883.81 | 103.1131 | 1883.81 | 141.2227 | 1883.81 | 112.5538 | 1883.81 | 105.8957 |  | 1883.81 | 108.8612 |
| 1883.56 | 21.97907 | 1884.42 | -97.2183 | 1884.43 | 88.08203 | 1884.43 | 102.1461 | 1884.43 | 136.6247 | 1884.43 | 111.7501 | 1884.43 | 101.1888 |  | 1884.43 | 105.7667 |
| 1884.18 | 22.53802 | 1885.03 | -97.4766 | 1885.04 | 85.39836 | 1885.04 | 99.39399 | 1885.04 | 131.9749 | 1885.04 | 109.1586 | 1885.04 | 96.43178 |  | 1885.04 | 103.3039 |
| 1884.79 | 23.09892 | 1885.65 | -96.8476 | 1885.65 | 83.66404 | 1885.65 | 96.79017 | 1885.65 | 128.201 | 1885.65 | 106.7154 | 1885.65 | 92.5508 |  | 1885.65 | 101.7905 |
| 1885.41 | 23.66375 | 1886.26 | -96.6994 | 1886.27 | 81.90178 | 1886.27 | 94.85862 | 1886.27 | 125.8468 | 1886.27 | 104.9471 | 1886.27 | 90.08767 |  | 1886.27 | 100.2527 |
| 1886.02 | 24.23491 | 1886.87 | -97.065 | 1886.88 | 79.57276 | 1886.88 | 92.90323 | 1886.88 | 123.0322 | 1886.88 | 103.1524 | 1886.88 | 87.16592 |  | 1886.88 | 98.14458 |
| 1886.63 | 24.81458 | 1887.49 | -96.8009 | 1887.5 | 77.36305 | 1887.5 | 90.03776 | 1887.5 | 120.368 | 1887.5 | 100.4502 | 1887.5 | 84.39279 |  | 1887.5 | 96.15938 |
| 1887.25 | 25.40279 | 1888.1 | -96.6207 | 1888.11 | 74.52455 | 1888.11 | 89.13423 | 1888.11 | 117.2421 | 1888.11 | 99.70731 | 1888.11 | 81.1598 |  | 1888.11 | 93.54177 |
| 1887.86 | 25.99943 | 1888.71 | -96.868 | 1888.72 | 71.61782 | 1888.72 | 86.32971 | 1888.72 | 112.6794 | 1888.72 | 97.06343 | 1888.72 | 76.48995 |  | 1888.72 | 90.85593 |
| 1888.48 | 26.60588 | 1889.33 | -97.6966 | 1889.34 | 69.29604 | 1889.34 | 83.72538 | 1889.34 | 108.1029 | 1889.34 | 94.62238 | 1889.34 | 71.80455 |  | 1889.34 | 88.75865 |
| 1889.09 | 27.2239 | 1889.94 | -98.4902 | 1889.95 | 68.19166 | 1889.95 | 82.00969 | 1889.95 | 104.1148 | 1889.95 | 93.06733 | 1889.95 | 67.70921 |  | 1889.95 | 87.87516 |
| 1889.71 | 27.85348 | 1890.55 | -98.0888 | 1890.56 | 66.16271 | 1890.56 | 79.92211 | 1890.56 | 99.97963 | 1890.56 | 91.1404 | 1890.56 | 63.46695 |  | 1890.56 | 86.0671 |
| 1890.32 | 28.49556 | 1891.16 | -97.2062 | 1891.18 | 65.09033 | 1891.18 | 77.98406 | 1891.18 | 97.67883 | 1891.18 | 89.36562 | 1891.18 | 61.05724 |  | 1891.18 | 85.21923 |
| 1890.93 | 29.15232 | 1891.78 | -97.5945 | 1891.79 | 63.83976 | 1891.79 | 76.61461 | 1891.79 | 93.98523 | 1891.79 | 88.15682 | 1891.79 | 57.2565 |  | 1891.79 | 84.18954 |
| 1891.55 | 29.82496 | 1892.39 | -98.5291 | 1892.4 | 61.73094 | 1892.4 | 74.94967 | 1892.4 | 91.37752 | 1892.4 | 86.65252 | 1892.4 | 54.54164 |  | 1892.4 | 82.30162 |
| 1892.16 | 30.51282 | 1893 | -98.6452 | 1893.02 | 59.97616 | 1893.02 | 73.33758 | 1893.02 | 88.69509 | 1893.02 | 85.20371 | 1893.02 | 51.7503 |  | 1893.02 | 80.77134 |
| 1892.77 | 31.21761 | 1893.62 | -98.2808 | 1893.63 | 58.49735 | 1893.63 | 72.02088 | 1893.63 | 85.61718 | 1893.63 | 84.04764 | 1893.63 | 48.56525 |  | 1893.63 | 79.51342 |
| 1893.39 | 31.94115 | 1894.23 | -98.4626 | 1894.24 | 57.56461 | 1894.24 | 71.29633 | 1894.24 | 83.90574 | 1894.24 | 83.48373 | 1894.24 | 46.74666 |  | 1894.24 | 78.80157 |
| 1894 | 32.68366 | 1894.84 | -98.7538 | 1894.85 | 56.85005 | 1894.85 | 70.425 | 1894.85 | 82.32856 | 1894.85 | 82.77304 | 1894.85 | 45.06233 |  | 1894.85 | 78.3079 |
| 1894.61 | 33.44628 | 1895.45 | -99.5317 | 1895.47 | 54.67011 | 1895.47 | 68.93025 | 1895.47 | 81.11039 | 1895.47 | 81.44157 | 1895.47 | 43.73526 |  | 1895.47 | 76.35247 |
| 1895.23 | 34.22826 | 1896.07 | -98.9764 | 1896.08 | 52.20255 | 1896.08 | 66.39979 | 1896.08 | 81.04257 | 1896.08 | 79.07175 | 1896.08 | 43.56029 |  | 1896.08 | 74.1058 |
| 1895.84 | 35.02818 | 1896.68 | -99.7715 | 1896.69 | 51.54362 | 1896.69 | 64.95658 | 1896.69 | 80.27788 | 1896.69 | 77.78919 | 1896.69 | 42.68845 |  | 1896.69 | 73.66775 |
| 1896.46 | 35.84532 | 1897.29 | -100.626 | 1897.31 | 50.61283 | 1897.31 | 63.40721 | 1897.31 | 81.0628 | 1897.31 | 76.40309 | 1897.31 | 43.36446 |  | 1897.31 | 72.96147 |
| 1897.07 | 36.67942 | 1897.9 | -101.417 | 1897.92 | 49.9488 | 1897.92 | 60.74851 | 1897.92 | 80.97733 | 1897.92 | 73.90503 | 1897.92 | 43.17185 |  | 1897.92 | 72.51833 |
| 1897.68 | 37.53034 | 1898.52 | -101.68 | 1898.53 | 48.95849 | 1898.53 | 60.64373 | 1898.53 | 79.00794 | 1898.53 | 73.9609 | 1898.53 | 41.09531 |  | 1898.53 | 71.74891 |
| 1898.3 | 38.39881 | 1899.13 | -102.398 | 1899.14 | 47.00382 | 1899.14 | 58.98629 | 1899.14 | 74.99104 | 1899.14 | 72.4641 | 1899.14 | 36.97126 |  | 1899.14 | 70.01512 |
| 1898.91 | 39.28377 | 1899.74 | -102.341 | 1899.76 | 45.35238 | 1899.76 | 55.95308 | 1899.76 | 72.16355 | 1899.76 | 69.59417 | 1899.76 | 34.03486 |  | 1899.76 | 68.5882 |
| 1899.52 | 40.18383 | 1900.35 | -103.278 | 1900.37 | 43.41999 | 1900.37 | 53.67141 | 1900.37 | 68.78091 | 1900.37 | 67.47314 | 1900.37 | 30.54508 |  | 1900.37 | 66.8767 |
| 1900.13 | 41.09678 | 1900.96 | -104.315 | 1900.98 | 41.92271 | 1900.98 | 51.17444 | 1900.98 | 67.49533 | 1900.98 | 65.13681 | 1900.98 | 29.15235 |  | 1900.98 | 65.6003 |
| 1900.75 | 42.02001 | 1901.58 | -105.378 | 1901.59 | 39.7764 | 1901.59 | 49.0512 | 1901.59 | 65.53681 | 1901.59 | 63.17422 | 1901.59 | 27.08668 |  | 1901.59 | 63.67488 |
| 1901.36 | 42.95217 | 1902.19 | -105.497 | 1902.21 | 38.99347 | 1902.21 | 45.89306 | 1902.21 | 62.22921 | 1902.21 | 60.17935 | 1902.21 | 23.67018 |  | 1902.21 | 63.11646 |
| 1901.97 | 43.89343 | 1902.8 | -105.061 | 1902.82 | 38.01554 | 1902.82 | 43.38069 | 1902.82 | 59.44573 | 1902.82 | 57.82762 | 1902.82 | 20.77955 |  | 1902.82 | 62.35942 |
| 1902.59 | 44.84462 | 1903.41 | -105.764 | 1903.43 | 36.41931 | 1903.43 | 41.53252 | 1903.43 | 55.75239 | 1903.43 | 56.14009 | 1903.43 | 16.97907 |  | 1903.43 | 60.98408 |
| 1903.2 | 45.80462 | 1904.02 | -104.368 | 1904.04 | 34.30974 | 1904.04 | 39.4716 | 1904.04 | 52.51494 | 1904.04 | 54.23981 | 1904.04 | 13.63447 |  | 1904.04 | 59.0954 |
| 1903.81 | 46.77108 | 1904.64 | -103.91 | 1904.65 | 33.13299 | 1904.65 | 37.34707 | 1904.65 | 50.17931 | 1904.65 | 52.27593 | 1904.65 | 11.19169 |  | 1904.65 | 58.13953 |
| 1904.42 | 47.74173 | 1905.25 | -104.248 | 1905.27 | 31.83961 | 1905.27 | 34.60293 | 1905.27 | 48.92851 | 1905.27 | 49.69506 | 1905.27 | 9.83199 |  | 1905.27 | 57.07066 |
| 1905.04 | 48.71559 | 1905.86 | -102.728 | 1905.88 | 30.51436 | 1905.88 | 32.47888 | 1905.88 | 47.98165 | 1905.88 | 47.73165 | 1905.88 | 8.77797 |  | 1905.88 | 55.9663 |
| 1905.65 | 49.6885 | 1906.47 | -103.296 | 1906.49 | 29.23381 | 1906.49 | 31.26698 | 1906.49 | 46.81361 | 1906.49 | 46.68039 | 1906.49 | 7.50279 |  | 1906.49 | 54.90664 |
| 1906.26 | 50.65566 | 1907.08 | -102.409 | 1907.1 | 27.38576 | 1907.1 | 29.82124 | 1907.1 | 44.94747 | 1907.1 | 45.3953 | 1907.1 | 5.5295 |  | 1907.1 | 53.27948 |
| 1906.87 | 51.61581 | 1907.69 | -101.399 | 1907.71 | 25.66123 | 1907.71 | 28.31413 | 1907.71 | 43.36487 | 1907.71 | 44.04883 | 1907.71 | 3.83975 |  | 1907.71 | 51.77584 |
| 1907.49 | 52.56827 | 1908.3 | -100.698 | 1908.32 | 24.30651 | 1908.32 | 26.21232 | 1908.32 | 40.20246 | 1908.32 | 42.10766 | 1908.32 | 0.57019 |  | 1908.32 | 50.64201 |
| 1908.1 | 53.51041 | 1908.92 | -100.349 | 1908.94 | 21.77184 | 1908.94 | 23.85187 | 1908.94 | 37.60822 | 1908.94 | 39.91049 | 1908.94 | -2.13295 |  | 1908.94 | 48.33184 |
| 1908.71 | 54.44071 | 1909.53 | -100.904 | 1909.55 | 20.16921 | 1909.55 | 22.72916 | 1909.55 | 35.96282 | 1909.55 | 38.94842 | 1909.55 | -3.8855 |  | 1909.55 | 46.95011 |
| 1909.32 | 55.35736 | 1910.14 | -99.9174 | 1910.16 | 19.13561 | 1910.16 | 21.10233 | 1910.16 | 32.96408 | 1910.16 | 37.48223 | 1910.16 | -6.99139 |  | 1910.16 | 46.13739 |
| 1909.94 | 56.25966 | 1910.75 | -101.868 | 1910.77 | 17.99926 | 1910.77 | 20.62883 | 1910.77 | 31.09318 | 1910.77 | 37.16937 | 1910.77 | -8.96943 |  | 1910.77 | 45.22193 |
| 1910.55 | 57.14665 | 1911.36 | -101.992 | 1911.38 | 16.6552 | 1911.38 | 19.99835 | 1911.38 | 30.0091 | 1911.38 | 36.69954 | 1911.38 | -10.1607 |  | 1911.38 | 44.09876 |
| 1911.16 | 58.0147 | 1911.97 | -101.262 | 1911.99 | 15.66174 | 1911.99 | 18.58749 | 1911.99 | 30.14089 | 1911.99 | 35.44932 | 1911.99 | -10.136 |  | 1911.99 | 43.32618 |
| 1911.77 | 58.86041 | 1912.58 | -101.858 | 1912.61 | 14.86347 | 1912.61 | 17.39105 | 1912.61 | 28.87503 | 1912.61 | 34.41615 | 1912.61 | -11.5108 |  | 1912.61 | 42.75243 |
| 1912.38 | 59.68281 | 1913.19 | -101.639 | 1913.22 | 15.08936 | 1913.22 | 17.99203 | 1913.22 | 28.15697 | 1913.22 | 35.17777 | 1913.22 | -12.336 |  | 1913.22 | 43.1992 |
| 1913 | 60.47971 | 1913.8 | -101.736 | 1913.83 | 14.58249 | 1913.83 | 16.39732 | 1913.83 | 28.54753 | 1913.83 | 33.74371 | 1913.83 | -12.0526 |  | 1913.83 | 42.91322 |
| 1913.61 | 61.24988 | 1914.42 | -102.287 | 1914.44 | 13.82661 | 1914.44 | 16.56497 | 1914.44 | 28.70673 | 1914.44 | 34.072 | 1914.44 | -12.0005 |  | 1914.44 | 42.37823 |
| 1914.22 | 61.99294 | 1915.03 | -102.872 | 1915.05 | 12.27838 | 1915.05 | 16.46889 | 1915.05 | 27.43396 | 1915.05 | 34.13657 | 1915.05 | -13.3805 |  | 1915.05 | 41.05089 |
| 1914.83 | 62.7082 | 1915.64 | -103.406 | 1915.66 | 12.25185 | 1915.66 | 14.8229 | 1915.66 | 25.78466 | 1915.66 | 32.65121 | 1915.66 | -15.1369 |  | 1915.66 | 41.24525 |
| 1915.44 | 63.39638 | 1916.25 | -102.609 | 1916.27 | 11.84532 | 1916.27 | 14.1069 | 1916.27 | 25.934 | 1916.27 | 32.09586 | 1916.27 | -15.0947 |  | 1916.27 | 41.05961 |
| 1916.05 | 64.05891 | 1916.86 | -102.609 | 1916.88 | 10.47736 | 1916.88 | 12.91981 | 1916.88 | 25.05877 | 1916.88 | 31.06941 | 1916.88 | -16.0771 |  | 1916.88 | 39.91253 |
| 1916.66 | 64.69677 | 1917.47 | -101.34 | 1917.49 | 10.29195 | 1917.49 | 11.81782 | 1917.49 | 23.10628 | 1917.49 | 30.12806 | 1917.49 | -18.1367 |  | 1917.49 | 39.94801 |
| 1917.28 | 65.3122 | 1918.08 | -102.263 | 1918.1 | 10.56648 | 1918.1 | 10.68454 | 1918.1 | 21.23354 | 1918.1 | 29.15542 | 1918.1 | -20.1166 |  | 1918.1 | 40.44343 |
| 1917.89 | 65.90527 | 1918.69 | -101.821 | 1918.71 | 9.33768 | 1918.71 | 10.02126 | 1918.71 | 19.75434 | 1918.71 | 28.65279 | 1918.71 | -21.703 |  | 1918.71 | 39.43551 |
| 1918.5 | 66.47704 | 1919.3 | -101.732 | 1919.32 | 9.22671 | 1919.32 | 7.97896 | 1919.32 | 17.91788 | 1919.32 | 26.77113 | 1919.32 | -23.6466 |  | 1919.32 | 39.54544 |
| 1919.11 | 67.0302 | 1919.91 | -102.005 | 1919.94 | 8.87899 | 1919.94 | 8.00912 | 1919.94 | 16.46729 | 1919.94 | 26.96457 | 1919.94 | -25.2061 |  | 1919.94 | 39.42223 |
| 1919.72 | 67.5646 | 1920.52 | -102.298 | 1920.55 | 8.58019 | 1920.55 | 6.8482 | 1920.55 | 15.62259 | 1920.55 | 25.96428 | 1920.55 | -26.1579 |  | 1920.55 | 39.34431 |
| 1920.33 | 68.07923 | 1921.13 | -101.831 | 1921.16 | 7.03544 | 1921.16 | 5.48892 | 1921.16 | 14.59627 | 1921.16 | 24.76565 | 1921.16 | -27.2914 |  | 1921.16 | 38.02045 |
| 1920.94 | 68.57535 | 1921.74 | -101.889 | 1921.77 | 6.94834 | 1921.77 | 6.01945 | 1921.77 | 12.57642 | 1921.77 | 25.45681 | 1921.77 | -29.4184 |  | 1921.77 | 38.15424 |
| 1921.55 | 69.04963 | 1922.35 | -101.526 | 1922.38 | 5.83046 | 1922.38 | 5.03527 | 1922.38 | 10.99461 | 1922.38 | 24.63328 | 1922.38 | -31.1073 |  | 1922.38 | 37.25724 |
| 1922.17 | 69.49675 | 1922.96 | -101.986 | 1922.99 | 3.39983 | 1922.99 | 4.31521 | 1922.99 | 10.43496 | 1922.99 | 24.07386 | 1922.99 | -31.7741 |  | 1922.99 | 35.0475 |
| 1922.78 | 69.91503 | 1923.57 | -101.859 | 1923.6 | 2.34469 | 1923.6 | 4.40103 | 1923.6 | 9.11687 | 1923.6 | 24.32032 | 1923.6 | -33.1994 |  | 1923.6 | 34.21325 |
| 1923.39 | 70.30565 | 1924.18 | -102.426 | 1924.21 | 2.27714 | 1924.21 | 3.37105 | 1924.21 | 8.76442 | 1924.21 | 23.45098 | 1924.21 | -33.659 |  | 1924.21 | 34.36659 |
| 1924 | 70.66644 | 1924.79 | -100.786 | 1924.82 | 2.09502 | 1924.82 | 1.77645 | 1924.82 | 7.23466 | 1924.82 | 22.01702 | 1924.82 | -35.2959 |  | 1924.82 | 34.40536 |
| 1924.61 | 70.99747 | 1925.4 | -100.593 | 1925.43 | 1.91133 | 1925.43 | 1.05635 | 1925.43 | 4.93921 | 1925.43 | 21.45757 | 1925.43 | -37.6985 |  | 1925.43 | 34.44255 |
| 1925.22 | 71.29923 | 1926.01 | -101.108 | 1926.04 | 0.6443 | 1926.04 | -0.21139 | 1926.04 | 3.2669 | 1926.04 | 20.35048 | 1926.04 | -39.4779 |  | 1926.04 | 33.39642 |
| 1925.83 | 71.57095 | 1926.62 | -99.7397 | 1926.65 | 0.72865 | 1926.65 | 0.1997 | 1926.65 | 2.55596 | 1926.65 | 20.9222 | 1926.65 | -40.296 |  | 1926.65 | 33.70166 |
| 1926.44 | 71.81097 | 1927.23 | -99.0661 | 1927.26 | 1.0079 | 1927.26 | 0.02262 | 1927.26 | 1.41659 | 1927.26 | 20.84452 | 1927.26 | -41.5425 |  | 1927.26 | 34.2018 |
| 1927.05 | 72.01906 | 1927.84 | -99.0424 | 1927.87 | 0.532 | 1927.87 | 0.45045 | 1927.87 | 0.13383 | 1927.87 | 21.05515 | 1927.87 | -42.9324 |  | 1927.87 | 33.94678 |
| 1927.66 | 72.19399 | 1928.45 | -98.8148 | 1928.48 | -0.09554 | 1928.48 | 1.217 | 1928.48 | -0.25348 | 1928.48 | 21.60449 | 1928.48 | -43.425 |  | 1928.48 | 33.54013 |
| 1928.27 | 72.33307 | 1929.06 | -99.4879 | 1929.09 | -0.47974 | 1929.09 | 2.48355 | 1929.09 | -1.07613 | 1929.09 | 22.65383 | 1929.09 | -44.3518 |  | 1929.09 | 33.37682 |
| 1928.88 | 72.43466 | 1929.67 | -99.4176 | 1929.7 | -0.84061 | 1929.7 | 2.0252 | 1929.7 | 0.44298 | 1929.7 | 21.97827 | 1929.7 | -42.9368 |  | 1929.7 | 33.23684 |
| 1929.49 | 72.49753 | 1930.27 | -99.7119 | 1930.31 | -1.07579 | 1930.31 | 2.93861 | 1930.31 | 3.40601 | 1930.31 | 22.67448 | 1930.31 | -40.078 |  | 1930.31 | 33.22254 |
| 1930.1 | 72.5194 | 1930.88 | -100.287 | 1930.92 | -1.37038 | 1930.92 | 4.40928 | 1930.92 | 4.84689 | 1930.92 | 23.92794 | 1930.92 | -38.7413 |  | 1930.92 | 33.14884 |
| 1930.71 | 72.49247 | 1931.49 | -100.968 | 1931.53 | -0.31307 | 1931.53 | 5.34572 | 1931.53 | 6.12124 | 1931.53 | 24.64717 | 1931.53 | -37.5711 |  | 1931.53 | 34.42703 |
| 1931.32 | 72.41681 | 1932.1 | -102.134 | 1932.13 | 0.71011 | 1932.13 | 6.27487 | 1932.13 | 8.15408 | 1932.13 | 25.36267 | 1932.13 | -35.6407 |  | 1932.13 | 35.44464 |
| 1931.93 | 72.29544 | 1932.71 | -102.411 | 1932.74 | 2.48308 | 1932.74 | 7.2615 | 1932.74 | 9.5947 | 1932.74 | 26.1321 | 1932.74 | -34.3043 |  | 1932.74 | 37.06637 |
| 1932.54 | 72.13211 | 1933.32 | -102.608 | 1933.35 | 3.86821 | 1933.35 | 8.47676 | 1933.35 | 11.8416 | 1933.35 | 27.13015 | 1933.35 | -32.1615 |  | 1933.35 | 38.30025 |
| 1933.15 | 71.93451 | 1933.93 | -103.631 | 1933.96 | 4.88314 | 1933.96 | 8.9128 | 1933.96 | 14.78654 | 1933.96 | 27.34898 | 1933.96 | -29.3208 |  | 1933.96 | 39.16393 |
| 1933.76 | 71.70448 | 1934.54 | -103.849 | 1934.57 | 5.91644 | 1934.57 | 10.54618 | 1934.57 | 15.22633 | 1934.57 | 28.76516 | 1934.57 | -28.9851 |  | 1934.57 | 40.04599 |
| 1934.37 | 71.44529 | 1935.15 | -103.92 | 1935.18 | 7.00013 | 1935.18 | 11.23054 | 1935.18 | 17.73592 | 1935.18 | 29.23231 | 1935.18 | -26.5797 |  | 1935.18 | 40.97844 |
| 1934.98 | 71.16443 | 1935.76 | -104.628 | 1935.79 | 8.27612 | 1935.79 | 12.17126 | 1935.79 | 20.36761 | 1935.79 | 29.95582 | 1935.79 | -24.0522 |  | 1935.79 | 42.10318 |
| 1935.59 | 70.86241 | 1936.36 | -105.062 | 1936.4 | 9.39759 | 1936.4 | 14.90629 | 1936.4 | 22.07009 | 1936.4 | 32.47365 | 1936.4 | -22.4539 |  | 1936.4 | 43.07342 |
| 1936.2 | 70.54093 | 1936.97 | -104.465 | 1937.01 | 10.09058 | 1937.01 | 16.83553 | 1937.01 | 24.32565 | 1937.01 | 34.18567 | 1937.01 | -20.3025 |  | 1937.01 | 43.61516 |
| 1936.81 | 70.20429 | 1937.58 | -104.564 | 1937.62 | 11.37258 | 1937.62 | 18.22182 | 1937.62 | 27.27866 | 1937.62 | 35.35476 | 1937.62 | -17.4537 |  | 1937.62 | 44.74592 |
| 1937.42 | 69.85439 | 1938.19 | -105.515 | 1938.23 | 13.36302 | 1938.23 | 19.15125 | 1938.23 | 31.03285 | 1938.23 | 36.06698 | 1938.23 | -13.8036 |  | 1938.23 | 46.58511 |
| 1938.03 | 69.49098 | 1938.8 | -104.412 | 1938.84 | 15.48536 | 1938.84 | 21.8984 | 1938.84 | 33.72188 | 1938.84 | 38.59693 | 1938.84 | -11.2188 |  | 1938.84 | 48.55621 |
| 1938.64 | 69.11517 | 1939.41 | -103.706 | 1939.44 | 17.77502 | 1939.44 | 24.67416 | 1939.44 | 37.36117 | 1939.44 | 41.15904 | 1939.44 | -7.68194 |  | 1939.44 | 50.69711 |
| 1939.25 | 68.72971 | 1940.02 | -104.5 | 1940.05 | 19.15932 | 1940.05 | 27.30955 | 1940.05 | 40.40491 | 1940.05 | 43.57722 | 1940.05 | -4.74237 |  | 1940.05 | 51.93016 |
| 1939.86 | 68.33293 | 1940.62 | -104.169 | 1940.66 | 21.5046 | 1940.66 | 28.60769 | 1940.66 | 43.39002 | 1940.66 | 44.65815 | 1940.66 | -1.86143 |  | 1940.66 | 54.1242 |
| 1940.47 | 67.92786 | 1941.23 | -103.535 | 1941.27 | 23.58178 | 1941.27 | 31.23081 | 1941.27 | 47.38018 | 1941.27 | 47.06407 | 1941.27 | 2.02456 |  | 1941.27 | 56.05013 |
| 1941.08 | 67.51943 | 1941.84 | -104.055 | 1941.88 | 25.04582 | 1941.88 | 32.48315 | 1941.88 | 49.72465 | 1941.88 | 48.0992 | 1941.88 | 4.26486 |  | 1941.88 | 57.36293 |
| 1941.68 | 67.11111 | 1942.45 | -103.623 | 1942.49 | 27.37319 | 1942.49 | 34.25765 | 1942.49 | 53.20069 | 1942.49 | 49.65649 | 1942.49 | 7.63673 |  | 1942.49 | 59.53906 |
| 1942.29 | 66.70406 | 1943.06 | -103.87 | 1943.09 | 29.7647 | 1943.09 | 36.62259 | 1943.09 | 55.44085 | 1943.09 | 51.80778 | 1943.09 | 9.77443 |  | 1943.09 | 61.7818 |
| 1942.9 | 66.30272 | 1943.66 | -103.978 | 1943.7 | 31.88025 | 1943.7 | 39.20148 | 1943.7 | 59.46566 | 1943.7 | 54.16947 | 1943.7 | 13.69507 |  | 1943.7 | 63.74611 |
| 1943.51 | 65.91131 | 1944.27 | -103.426 | 1944.31 | 34.1207 | 1944.31 | 40.62704 | 1944.31 | 63.52105 | 1944.31 | 55.37782 | 1944.31 | 17.64629 |  | 1944.31 | 65.83532 |
| 1944.12 | 65.53197 | 1944.88 | -103.062 | 1944.92 | 35.99658 | 1944.92 | 43.60915 | 1944.92 | 65.86855 | 1944.92 | 58.14272 | 1944.92 | 19.88962 |  | 1944.92 | 67.55996 |
| 1944.73 | 65.16838 | 1945.49 | -103.63 | 1945.53 | 36.86933 | 1945.53 | 44.14067 | 1945.53 | 68.14409 | 1945.53 | 58.45704 | 1945.53 | 22.06099 |  | 1945.53 | 68.28146 |
| 1945.34 | 64.82232 | 1946.1 | -103.487 | 1946.14 | 39.50776 | 1946.14 | 47.01651 | 1946.14 | 73.07727 | 1946.14 | 61.11567 | 1946.14 | 26.89 |  | 1946.14 | 70.76865 |
| 1945.95 | 64.49364 | 1946.7 | -102.766 | 1946.74 | 41.51234 | 1946.74 | 50.57702 | 1946.74 | 77.40836 | 1946.74 | 64.46253 | 1946.74 | 31.11863 |  | 1946.74 | 72.62447 |
| 1946.55 | 64.17819 | 1947.31 | -103.07 | 1947.35 | 44.21836 | 1947.35 | 53.12804 | 1947.35 | 80.83384 | 1947.35 | 66.79634 | 1947.35 | 34.43994 |  | 1947.35 | 75.17925 |
| 1947.16 | 63.87512 | 1947.92 | -104.23 | 1947.96 | 46.34935 | 1947.96 | 55.06231 | 1947.96 | 84.79114 | 1947.96 | 68.5134 | 1947.96 | 38.29307 |  | 1947.96 | 77.15898 |
| 1947.77 | 63.58364 | 1948.53 | -104.512 | 1948.57 | 47.06831 | 1948.57 | 55.77999 | 1948.57 | 88.01898 | 1948.57 | 69.01388 | 1948.57 | 41.41674 |  | 1948.57 | 77.7267 |
| 1948.38 | 63.30233 | 1949.13 | -104.568 | 1949.18 | 48.07413 | 1949.18 | 58.19081 | 1949.18 | 93.2974 | 1949.18 | 71.2075 | 1949.18 | 46.591 |  | 1949.18 | 78.58128 |
| 1948.99 | 63.03704 | 1949.74 | -104.203 | 1949.78 | 50.7114 | 1949.78 | 61.51611 | 1949.78 | 98.14608 | 1949.78 | 74.31915 | 1949.78 | 51.33721 |  | 1949.78 | 81.06978 |
| 1949.6 | 62.78985 | 1950.35 | -104.14 | 1950.39 | 52.48442 | 1950.39 | 64.02447 | 1950.39 | 102.6231 | 1950.39 | 76.6103 | 1950.39 | 55.71004 |  | 1950.39 | 82.69156 |
| 1950.2 | 62.56267 | 1950.96 | -103.473 | 1951 | 54.29018 | 1951 | 65.35478 | 1951 | 106.7232 | 1951 | 77.72341 | 1951 | 59.706 |  | 1951 | 84.34608 |
| 1950.81 | 62.35888 | 1951.56 | -103.006 | 1951.61 | 57.75928 | 1951.61 | 67.57765 | 1951.61 | 111.6281 | 1951.61 | 79.72906 | 1951.61 | 64.50667 |  | 1951.61 | 87.66393 |
| 1951.42 | 62.17662 | 1952.17 | -103.033 | 1952.21 | 59.97231 | 1952.21 | 68.79586 | 1952.21 | 116.4627 | 1952.21 | 80.73363 | 1952.21 | 69.23886 |  | 1952.21 | 89.7282 |
| 1952.03 | 62.01244 | 1952.78 | -102.644 | 1952.82 | 61.59409 | 1952.82 | 69.71782 | 1952.82 | 120.5038 | 1952.82 | 81.43839 | 1952.82 | 73.17575 |  | 1952.82 | 91.19874 |
| 1952.64 | 61.86152 | 1953.38 | -102.046 | 1953.43 | 62.73836 | 1953.43 | 70.55929 | 1953.43 | 124.1016 | 1953.43 | 82.06264 | 1953.43 | 76.66945 |  | 1953.43 | 92.19177 |
| 1953.25 | 61.72206 | 1953.99 | -101.046 | 1954.03 | 65.64329 | 1954.03 | 72.12287 | 1954.03 | 127.5647 | 1954.03 | 83.41258 | 1954.03 | 80.03001 |  | 1954.03 | 94.94793 |
| 1953.85 | 61.59146 | 1954.6 | -100.808 | 1954.64 | 67.78952 | 1954.64 | 73.35022 | 1954.64 | 132.4088 | 1954.64 | 84.42272 | 1954.64 | 84.76999 |  | 1954.64 | 96.94292 |
| 1954.46 | 61.46582 | 1955.21 | -99.9548 | 1955.25 | 68.84988 | 1955.25 | 75.74187 | 1955.25 | 135.4233 | 1955.25 | 86.59717 | 1955.25 | 87.68035 |  | 1955.25 | 97.85203 |
| 1955.07 | 61.34048 | 1955.81 | -99.0336 | 1955.86 | 71.03023 | 1955.86 | 77.52196 | 1955.86 | 139.7253 | 1955.86 | 88.16005 | 1955.86 | 91.87817 |  | 1955.86 | 99.88114 |
| 1955.68 | 61.20618 | 1956.42 | -98.9743 | 1956.46 | 71.51529 | 1956.46 | 78.60916 | 1956.46 | 144.4444 | 1956.46 | 89.0336 | 1956.46 | 96.49475 |  | 1956.46 | 100.2174 |
| 1956.29 | 61.05608 | 1957.02 | -98.8536 | 1957.07 | 72.64774 | 1957.07 | 80.19776 | 1957.07 | 147.6347 | 1957.07 | 90.405 | 1957.07 | 99.58095 |  | 1957.07 | 101.1986 |
| 1956.89 | 60.88622 | 1957.63 | -100.153 | 1957.68 | 73.65719 | 1957.68 | 81.66076 | 1957.68 | 151.0927 | 1957.68 | 91.65079 | 1957.68 | 102.9347 |  | 1957.68 | 102.0569 |
| 1957.5 | 60.69128 | 1958.24 | -100.43 | 1958.28 | 73.25984 | 1958.28 | 82.88255 | 1958.28 | 154.7048 | 1958.28 | 92.65893 | 1958.28 | 106.4444 |  | 1958.28 | 101.5107 |
| 1958.11 | 60.46236 | 1958.85 | -101.523 | 1958.89 | 73.95719 | 1958.89 | 84.87253 | 1958.89 | 156.2981 | 1958.89 | 94.4317 | 1958.89 | 107.9335 |  | 1958.89 | 102.0568 |
| 1958.72 | 60.19052 | 1959.45 | -101.72 | 1959.5 | 75.06762 | 1959.5 | 86.12964 | 1959.5 | 157.9608 | 1959.5 | 95.47161 | 1959.5 | 109.492 |  | 1959.5 | 103.016 |
| 1959.32 | 59.86942 | 1960.06 | -102.132 | 1960.1 | 74.98694 | 1960.1 | 87.0332 | 1960.1 | 157.7061 | 1960.1 | 96.16152 | 1960.1 | 109.1348 |  | 1960.1 | 102.7866 |
| 1959.93 | 59.49404 | 1960.66 | -103.581 | 1960.71 | 75.29613 | 1960.71 | 88.16334 | 1960.71 | 158.8757 | 1960.71 | 97.07445 | 1960.71 | 110.2003 |  | 1960.71 | 102.9445 |
| 1960.54 | 59.06082 | 1961.27 | -103.629 | 1961.32 | 77.22257 | 1961.32 | 88.00034 | 1961.32 | 159.085 | 1961.32 | 96.69425 | 1961.32 | 110.3054 |  | 1961.32 | 104.7197 |
| 1961.14 | 58.56875 | 1961.88 | -103.765 | 1961.93 | 78.33092 | 1961.93 | 88.47527 | 1961.93 | 160.4493 | 1961.93 | 96.95197 | 1961.93 | 111.5656 |  | 1961.93 | 105.6768 |
| 1961.75 | 58.01845 | 1962.48 | -103.896 | 1962.53 | 77.87999 | 1962.53 | 88.67675 | 1962.53 | 160.2635 | 1962.53 | 96.9398 | 1962.53 | 111.2774 |  | 1962.53 | 105.0771 |
| 1962.36 | 57.40677 | 1963.09 | -104.044 | 1963.14 | 77.88539 | 1963.14 | 89.28482 | 1963.14 | 159.8579 | 1963.14 | 97.33066 | 1963.14 | 110.7675 |  | 1963.14 | 104.9313 |
| 1962.97 | 56.73008 | 1963.7 | -104.898 | 1963.74 | 78.27969 | 1963.74 | 89.75972 | 1963.74 | 160.563 | 1963.74 | 97.59191 | 1963.74 | 111.3702 |  | 1963.74 | 105.1768 |
| 1963.57 | 55.98931 | 1964.3 | -105.084 | 1964.35 | 77.43112 | 1964.35 | 89.88335 | 1964.35 | 159.4055 | 1964.35 | 97.49834 | 1964.35 | 110.1085 |  | 1964.35 | 104.177 |
| 1964.18 | 55.18205 | 1964.91 | -104.593 | 1964.96 | 76.5794 | 1964.96 | 90.14033 | 1964.96 | 158.7702 | 1964.96 | 97.53811 | 1964.96 | 109.369 |  | 1964.96 | 103.1741 |
| 1964.79 | 54.31591 | 1965.51 | -102.78 | 1965.56 | 76.76247 | 1965.56 | 90.31786 | 1965.56 | 160.6421 | 1965.56 | 97.50199 | 1965.56 | 111.1385 |  | 1965.56 | 103.2084 |
| 1965.39 | 53.39758 | 1966.12 | -102.477 | 1966.17 | 75.3635 | 1966.17 | 90.73012 | 1966.17 | 159.0095 | 1966.17 | 97.69705 | 1966.17 | 109.4018 |  | 1966.17 | 101.6582 |
| 1966 | 52.43535 | 1966.72 | -102.937 | 1966.78 | 73.29212 | 1966.78 | 90.62169 | 1966.78 | 157.9863 | 1966.78 | 97.3714 | 1966.78 | 108.2743 |  | 1966.78 | 99.43552 |
| 1966.61 | 51.43779 | 1967.33 | -102.651 | 1967.38 | 72.1859 | 1967.38 | 89.62714 | 1967.38 | 155.8351 | 1967.38 | 96.16321 | 1967.38 | 106.0207 |  | 1967.38 | 98.18055 |
| 1967.21 | 50.41558 | 1967.94 | -102.123 | 1967.99 | 72.43707 | 1967.99 | 88.39851 | 1967.99 | 153.4089 | 1967.99 | 94.71737 | 1967.99 | 103.4903 |  | 1967.99 | 98.28047 |
| 1967.82 | 49.38137 | 1968.54 | -101.939 | 1968.59 | 71.25394 | 1968.59 | 86.00071 | 1968.59 | 151.3464 | 1968.59 | 92.10593 | 1968.59 | 101.3254 |  | 1968.59 | 96.94857 |
| 1968.43 | 48.34131 | 1969.15 | -101.827 | 1969.2 | 70.54446 | 1969.2 | 86.02765 | 1969.2 | 150.4688 | 1969.2 | 91.91566 | 1969.2 | 100.3436 |  | 1969.2 | 96.08785 |
| 1969.03 | 47.3053 | 1969.75 | -101.816 | 1969.81 | 69.52341 | 1969.81 | 84.23851 | 1969.81 | 147.9961 | 1969.81 | 89.90932 | 1969.81 | 97.76672 |  | 1969.81 | 94.91556 |
| 1969.64 | 46.28472 | 1970.36 | -100.98 | 1970.41 | 68.72871 | 1970.41 | 82.0417 | 1970.41 | 146.1711 | 1970.41 | 87.49886 | 1970.41 | 95.83925 |  | 1970.41 | 93.97209 |
| 1970.25 | 45.28658 | 1970.96 | -99.8931 | 1971.02 | 70.17544 | 1971.02 | 81.4548 | 1971.02 | 145.2266 | 1971.02 | 86.69475 | 1971.02 | 94.79056 |  | 1971.02 | 95.26758 |
| 1970.85 | 44.31605 | 1971.57 | -99.8891 | 1971.62 | 69.81617 | 1971.62 | 79.86611 | 1971.62 | 142.8817 | 1971.62 | 84.89241 | 1971.62 | 92.34323 |  | 1971.62 | 94.75955 |
| 1971.46 | 43.3717 | 1972.17 | -100.719 | 1972.23 | 69.67859 | 1972.23 | 76.86313 | 1972.23 | 140.0272 | 1972.23 | 81.67223 | 1972.23 | 89.38453 |  | 1972.23 | 94.47073 |
| 1972.07 | 42.45092 | 1972.78 | -101.258 | 1972.83 | 68.73926 | 1972.83 | 76.5053 | 1972.83 | 138.7405 | 1972.83 | 81.10075 | 1972.83 | 87.99539 |  | 1972.83 | 93.38263 |
| 1972.67 | 41.55809 | 1973.38 | -101.597 | 1973.44 | 66.43593 | 1973.44 | 74.69084 | 1973.44 | 136.2642 | 1973.44 | 79.06908 | 1973.44 | 85.41487 |  | 1973.44 | 90.92806 |
| 1973.28 | 40.69936 | 1973.99 | -101.137 | 1974.05 | 64.68026 | 1974.05 | 72.54853 | 1974.05 | 134.437 | 1974.05 | 76.70957 | 1974.05 | 83.48357 |  | 1974.05 | 89.02114 |
| 1973.88 | 39.87071 | 1974.6 | -100.775 | 1974.65 | 63.40504 | 1974.65 | 70.42208 | 1974.65 | 131.7737 | 1974.65 | 74.36947 | 1974.65 | 80.71776 |  | 1974.65 | 87.59716 |
| 1974.49 | 39.06846 | 1975.2 | -101.666 | 1975.26 | 61.43911 | 1975.26 | 68.63593 | 1975.26 | 129.2065 | 1975.26 | 72.36611 | 1975.26 | 78.0464 |  | 1975.26 | 85.47998 |
| 1975.1 | 38.29129 | 1975.81 | -101.394 | 1975.86 | 59.2807 | 1975.86 | 67.60231 | 1975.86 | 127.7966 | 1975.86 | 71.11884 | 1975.86 | 76.53407 |  | 1975.86 | 83.17281 |
| 1975.7 | 37.53732 | 1976.41 | -101.484 | 1976.47 | 59.24672 | 1976.47 | 67.0544 | 1976.47 | 124.5888 | 1976.47 | 70.35372 | 1976.47 | 73.22212 |  | 1976.47 | 82.98759 |
| 1976.31 | 36.80673 | 1977.02 | -102 | 1977.07 | 57.97021 | 1977.07 | 64.93614 | 1977.07 | 120.0711 | 1977.07 | 68.02183 | 1977.07 | 68.60189 |  | 1977.07 | 81.56232 |
| 1976.91 | 36.10192 | 1977.62 | -101.034 | 1977.68 | 56.13638 | 1977.68 | 62.26616 | 1977.68 | 117.2554 | 1977.68 | 65.13463 | 1977.68 | 65.68205 |  | 1977.68 | 79.57724 |
| 1977.52 | 35.42158 | 1978.22 | -100.198 | 1978.28 | 55.37732 | 1978.28 | 60.40262 | 1978.28 | 113.4251 | 1978.28 | 63.05744 | 1978.28 | 61.74926 |  | 1978.28 | 78.66941 |
| 1978.12 | 34.7544 | 1978.83 | -101.329 | 1978.89 | 53.7993 | 1978.89 | 58.72624 | 1978.89 | 109.0256 | 1978.89 | 61.16386 | 1978.89 | 57.24564 |  | 1978.89 | 76.94016 |
| 1978.73 | 34.09064 | 1979.43 | -101.173 | 1979.49 | 52.47573 | 1979.49 | 58.06466 | 1979.49 | 107.7375 | 1979.49 | 60.28863 | 1979.49 | 55.85502 |  | 1979.49 | 75.46782 |
| 1979.34 | 33.42477 | 1980.04 | -101.063 | 1980.1 | 51.47027 | 1980.1 | 56.1477 | 1980.1 | 103.3759 | 1980.1 | 58.15447 | 1980.1 | 51.38924 |  | 1980.1 | 74.31111 |
| 1979.94 | 32.75102 | 1980.64 | -100.613 | 1980.7 | 49.27305 | 1980.7 | 53.5051 | 1980.7 | 99.84543 | 1980.7 | 55.29822 | 1980.7 | 47.75635 |  | 1980.7 | 71.96513 |
| 1980.55 | 32.07364 | 1981.25 | -102.129 | 1981.31 | 47.88955 | 1981.31 | 52.05657 | 1981.31 | 97.3097 | 1981.31 | 53.63249 | 1981.31 | 45.11645 |  | 1981.31 | 70.43038 |
| 1981.15 | 31.39408 | 1981.85 | -101.336 | 1981.91 | 47.47076 | 1981.91 | 50.06496 | 1981.91 | 93.70731 | 1981.91 | 51.42723 | 1981.91 | 41.4116 |  | 1981.91 | 69.86283 |
| 1981.76 | 30.71277 | 1982.46 | -102.417 | 1982.52 | 44.90459 | 1982.52 | 48.79091 | 1982.52 | 92.07187 | 1982.52 | 49.93597 | 1982.52 | 39.67199 |  | 1982.52 | 67.14542 |
| 1982.36 | 30.02626 | 1983.06 | -102.844 | 1983.12 | 42.85972 | 1983.12 | 47.80812 | 1983.12 | 88.37693 | 1983.12 | 48.73953 | 1983.12 | 35.87458 |  | 1983.12 | 64.95179 |
| 1982.97 | 29.32979 | 1983.66 | -103.221 | 1983.72 | 41.26872 | 1983.72 | 46.52188 | 1983.72 | 85.51703 | 1983.72 | 47.23965 | 1983.72 | 32.91223 |  | 1983.72 | 63.21202 |
| 1983.57 | 28.63177 | 1984.27 | -104.19 | 1984.33 | 38.82039 | 1984.33 | 45.01979 | 1984.33 | 81.28061 | 1984.33 | 45.52035 | 1984.33 | 28.57163 |  | 1984.33 | 60.61245 |
| 1984.18 | 27.93463 | 1984.87 | -105.81 | 1984.93 | 35.48023 | 1984.93 | 41.73598 | 1984.93 | 74.87657 | 1984.93 | 42.0229 | 1984.93 | 22.06513 |  | 1984.93 | 57.12353 |
| 1984.78 | 27.24164 | 1985.48 | -103.975 | 1985.54 | 32.69195 | 1985.54 | 38.74802 | 1985.54 | 69.25742 | 1985.54 | 38.81773 | 1985.54 | 16.34182 |  | 1985.54 | 54.18401 |
| 1985.39 | 26.55994 | 1986.08 | -104.435 | 1986.14 | 29.79874 | 1986.14 | 36.70816 | 1986.14 | 63.34985 | 1986.14 | 36.56422 | 1986.14 | 10.33178 |  | 1986.14 | 51.14203 |
| 1985.99 | 25.89334 | 1986.68 | -104.204 | 1986.75 | 27.60923 | 1986.75 | 32.96973 | 1986.75 | 58.15081 | 1986.75 | 32.60858 | 1986.75 | 5.02857 |  | 1986.75 | 48.80128 |
| 1986.6 | 25.23387 | 1987.29 | -104.718 | 1987.35 | 26.50903 | 1987.35 | 29.65216 | 1987.35 | 52.17708 | 1987.35 | 29.07736 | 1987.35 | -1.04762 |  | 1987.35 | 47.55231 |
| 1987.2 | 24.55935 | 1987.89 | -104.747 | 1987.95 | 23.64387 | 1987.95 | 26.62101 | 1987.95 | 47.88316 | 1987.95 | 25.83257 | 1987.95 | -5.444 |  | 1987.95 | 44.53839 |
| 1987.81 | 23.84006 | 1988.5 | -104.896 | 1988.56 | 20.36599 | 1988.56 | 24.3552 | 1988.56 | 42.87485 | 1988.56 | 23.34956 | 1988.56 | -10.5565 |  | 1988.56 | 41.10926 |
| 1988.41 | 23.05457 | 1989.1 | -104.746 | 1989.16 | 18.29363 | 1989.16 | 21.84925 | 1989.16 | 38.71449 | 1989.16 | 20.62995 | 1989.16 | -14.8193 |  | 1989.16 | 38.88815 |
| 1989.02 | 22.20553 | 1989.7 | -105.126 | 1989.77 | 15.90343 | 1989.77 | 18.94314 | 1989.77 | 35.45429 | 1989.77 | 17.50664 | 1989.77 | -18.1837 |  | 1989.77 | 36.34669 |
| 1989.62 | 21.28535 | 1990.31 | -105.011 | 1990.37 | 14.77944 | 1990.37 | 17.48848 | 1990.37 | 32.91481 | 1990.37 | 15.83833 | 1990.37 | -20.8256 |  | 1990.37 | 35.07394 |
| 1990.23 | 20.28494 | 1990.91 | -104.956 | 1990.97 | 14.04744 | 1990.97 | 13.69334 | 1990.97 | 28.62627 | 1990.97 | 11.82954 | 1990.97 | -25.2166 |  | 1990.97 | 34.19318 |
| 1990.83 | 19.19303 | 1991.51 | -105.55 | 1991.58 | 14.98998 | 1991.58 | 10.64704 | 1991.58 | 27.60543 | 1991.58 | 8.56604 | 1991.58 | -26.3416 |  | 1991.58 | 34.98448 |
| 1991.43 | 18.00529 | 1992.12 | -107.014 | 1992.18 | 14.41008 | 1992.18 | 10.55941 | 1992.18 | 26.0388 | 1992.18 | 8.26476 | 1992.18 | -28.0107 |  | 1992.18 | 34.25581 |
| 1992.04 | 16.72056 | 1992.72 | -108.815 | 1992.79 | 12.52218 | 1992.79 | 8.16707 | 1992.79 | 22.85992 | 1992.79 | 5.65522 | 1992.79 | -31.2938 |  | 1992.79 | 32.21667 |
| 1992.64 | 15.35012 | 1993.32 | -109.149 | 1993.39 | 8.00817 | 1993.39 | 8.10162 | 1993.39 | 18.46433 | 1993.39 | 5.37612 | 1993.39 | -35.7918 |  | 1993.39 | 27.55389 |
| 1993.25 | 13.89374 | 1993.93 | -109.321 | 1993.99 | 3.55185 | 1993.99 | 9.44388 | 1993.99 | 16.55566 | 1993.99 | 6.50473 | 1993.99 | -37.803 |  | 1993.99 | 22.94881 |
| 1993.85 | 12.27921 | 1994.53 | -108.772 | 1994.6 | 3.7883 | 1994.6 | 6.84911 | 1994.6 | 11.1953 | 1994.6 | 3.69275 | 1994.6 | -43.2675 |  | 1994.6 | 23.03402 |
| 1994.46 | 10.35459 | 1995.13 | -108.449 | 1995.2 | 2.95543 | 1995.2 | 5.32139 | 1995.2 | 7.34496 | 1995.2 | 1.95139 | 1995.2 | -47.2203 |  | 1995.2 | 22.05238 |
| 1995.06 | 8.19087 | 1995.74 | -108.628 | 1995.8 | 5.83184 | 1995.8 | 4.96759 | 1995.8 | 5.31654 | 1995.8 | 1.38394 | 1995.8 | -49.3512 |  | 1995.8 | 24.78003 |
| 1995.66 | 5.76487 | 1996.34 | -108.58 | 1996.41 | 4.80868 | 1996.41 | 0.97263 | 1996.41 | 7.5778 | 1996.41 | -2.82823 | 1996.41 | -47.1941 |  | 1996.41 | 23.60563 |
| 1996.27 | 2.91393 | 1996.94 | -109.248 | 1997.01 | 0.79261 | 1997.01 | -0.26865 | 1997.01 | 5.56061 | 1997.01 | -4.28315 | 1997.01 | -49.3137 |  | 1997.01 | 19.44079 |
| 1996.87 | -0.66532 | 1997.54 | -109.601 | 1997.61 | 1.36503 | 1997.61 | 0.20946 | 1997.61 | 7.6447 | 1997.61 | -4.01869 | 1997.61 | -47.3321 |  | 1997.61 | 19.86445 |
| 1997.47 | -4.85316 | 1998.15 | -107.611 | 1998.22 | 0 | 1998.22 | ###### | 1998.22 | 0 | 1998.22 | -4.44536 | 1998.22 | -55.081 |  | 1998.22 | 18.34817 |
| 1998.08 | -8.65377 | 1998.75 | -108.395 | 1998.82 | -18.046 | 1998.82 | -4.35468 | 1998.82 | -10.522 | 1998.82 | -9.01368 | 1998.82 | -65.7055 |  | 1998.82 | 0.15344 |
| 1998.68 | -13.5544 | 1999.35 | -111.372 | 1999.42 | -30.753 | 1999.42 | -18.7857 | 1999.42 | -71.4867 | 1999.42 | -23.6584 | 1999.42 | -126.773 |  | 1999.42 | -12.7023 |
| 1999.29 | -21.9084 | 1999.96 | -113.807 | 1999.45 | -62.5585 | 1999.45 | -64.2143 | 1999.45 | -151.167 | 1999.45 | -69.0976 | 1999.45 | -206.458 |  | 1999.45 | -44.5153 |

Table S6. Eccentricity statistics of different groups of NPs.

| Commercialized NPs |  |  |  |  |  | Self-made NPs |  |  |  |  |  | Naturally-derived NPs |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Area | Angle | Size (length) | Size (width) | Eccentricity |  | Area | Angle | Size (length) | Size (width) | Eccentricity |  | Area | Angle | Size (length) | Size (width) | Eccentricity |
| 1 | 128.4269 | 65.2738 | 33.45203 | 1.951266 | 0.737356 | 1 | 51.12323 | 211.8909 | 180.4325 | 1.17435 | 0.274888 | 1 | 83.92727 | 217.3941 | 186.4578 | 1.165916 | 0.26436 |
| 2 | 27.60772 | 74.32281 | 26.30844 | 2.825056 | 0.874701 | 2 | 9.49547 | 84.10376 | 57.80521 | 1.454951 | 0.527607 | 2 | 130.3198 | 186.1384 | 186.061 | 1.000416 | 0.000831 |
| 3 | 120.8743 | 59.16776 | 25.69424 | 2.302764 | 0.811418 | 3 | 76.8485 | 55.00751 | 48.01135 | 1.145719 | 0.238195 | 3 | 102.8392 | 200.769 | 160.6791 | 1.249503 | 0.359491 |
| 4 | 90 | 37 | 35 | 1.057143 | 0.105186 | 4 | 127.0528 | 67.97177 | 47.68233 | 1.425513 | 0.507895 | 4 | 122.2697 | 174.5122 | 117.2835 | 1.487952 | 0.548329 |
| 5 | 180 | 35.00006 | 35 | 1.000002 | 3.43E-06 | 5 | 117.2407 | 60.17126 | 32.23199 | 1.866818 | 0.713057 | 5 | 160.3207 | 135.4504 | 82.51981 | 1.641429 | 0.628845 |
| 6 | 180 | 35 | 35 | 1 | 0 | 6 | 179.2176 | 65.34293 | 30.57831 | 2.136905 | 0.781007 | 6 | 52.42703 | 103.4639 | 86.50756 | 1.19601 | 0.300914 |
| 7 | 180 | 35 | 35 | 1 | 0 | 7 | 125.4936 | 63.25586 | 29.54495 | 2.141004 | 0.781845 | 7 | 178.9376 | 126.958 | 76.95386 | 1.649794 | 0.632599 |
| 8 | 180 | 35 | 35 | 1 | 0 | 8 | 133.7276 | 47.81686 | 39.33096 | 1.215756 | 0.323439 | 8 | 78.62955 | 100.0857 | 69.9523 | 1.430771 | 0.511505 |
| 9 | 90 | 35 | 35 | 1 | 0 | 9 | 176.3997 | 54.09052 | 31.90146 | 1.69555 | 0.652161 | 9 | 160.9083 | 87.78128 | 69.75525 | 1.258418 | 0.368534 |
| 10 | 90 | 35 | 33 | 1.060606 | 0.11102 | 10 | 74.6982 | 43.3587 | 33.94877 | 1.27718 | 0.38695 | 10 | 15.91475 | 116.4319 | 66.86866 | 1.741203 | 0.670162 |
| 11 | 132.614 | 33.41129 | 32.85195 | 1.017026 | 0.033202 | 11 | 4.04107 | 55.36055 | 28.27698 | 1.957796 | 0.739105 | 11 | 23.30879 | 106.4246 | 47.04959 | 2.261967 | 0.804554 |
| 12 | 90 | 33 | 33 | 1 | 0 | 12 | 117.6666 | 53.39777 | 27.70023 | 1.927701 | 0.730896 | 12 | 102.8152 | 94.65283 | 68.75485 | 1.376671 | 0.472358 |
| 13 | 90 | 33 | 33 | 1 | 0 | 13 | 101.2473 | 44.72424 | 39.46472 | 1.133271 | 0.221368 | 13 | 153.4441 | 81.53949 | 68.06934 | 1.197889 | 0.303105 |
| 14 | 90 | 33 | 33 | 1 | 0 | 14 | 66.29077 | 46.22705 | 34.49014 | 1.340298 | 0.44333 | 14 | 29.59531 | 74.56863 | 64.021 | 1.164753 | 0.26289 |
| 15 | 1.82661 | 33.20636 | 31.20737 | 1.064055 | 0.116774 | 15 | 129.0647 | 61.29134 | 22.61447 | 2.710271 | 0.863863 | 15 | 71.86674 | 74.22833 | 60.15659 | 1.233919 | 0.343209 |
| 16 | 90 | 33 | 31 | 1.064516 | 0.117539 | 16 | 61.56537 | 47.65765 | 31.7811 | 1.499559 | 0.555294 | 16 | 149.6993 | 68.63689 | 61.77428 | 1.111092 | 0.189972 |
| 17 | 180 | 31 | 31 | 1 | 0 | 17 | 27.19413 | 55.65302 | 26.50879 | 2.099418 | 0.773117 | 17 | 7.31762 | 88.64755 | 74.69009 | 1.186872 | 0.290108 |
| 18 | 27.82318 | 42.57324 | 21.54422 | 1.976086 | 0.743913 | 18 | 29.12935 | 54.22849 | 28.71759 | 1.888337 | 0.719559 | 18 | 145.0721 | 68.81534 | 57.40659 | 1.198736 | 0.30409 |
| 19 | 0.56423 | 31.06743 | 29.06752 | 1.068802 | 0.124602 | 19 | 13.64577 | 55.28436 | 29.31073 | 1.886147 | 0.718908 | 19 | 43.92063 | 64.85364 | 50.79453 | 1.276784 | 0.38657 |
| 20 | 0.56423 | 31.06741 | 29.06754 | 1.068801 | 0.1246 | 20 | 88.59671 | 51.42648 | 28.30042 | 1.817163 | 0.697161 | 20 | 16.3725 | 77.38788 | 47.38191 | 1.633279 | 0.625131 |
| 21 | 90 | 29 | 29 | 1 | 0 | 21 | 21.02803 | 39.13531 | 30.20001 | 1.295871 | 0.404507 | 21 | 17.02202 | 73.79276 | 49.64342 | 1.486456 | 0.547419 |
| 22 | 154.9549 | 35.88318 | 19.33833 | 1.855547 | 0.70956 | 22 | 173.4573 | 54.54279 | 23.73816 | 2.297684 | 0.810583 | 22 | 128.0552 | 55.60815 | 52.72107 | 1.054761 | 0.101141 |
| 23 | 90 | 27 | 25 | 1.08 | 0.142661 | 23 | 38.32611 | 44.13373 | 30.89274 | 1.428612 | 0.510028 | 23 | 39.30696 | 67.32397 | 41.52016 | 1.621477 | 0.619654 |
| 24 | 180 | 25 | 25 | 1 | 0 | 24 | 16.7252 | 50.83078 | 25.91959 | 1.961095 | 0.739982 | 24 | 173.9936 | 70.11243 | 54.06686 | 1.296773 | 0.405335 |
| 25 | 90 | 21 | 21 | 1 | 0 | 25 | 132.8259 | 42.55606 | 29.49478 | 1.442834 | 0.519639 | 25 | 9.10801 | 57.07234 | 52.03988 | 1.096704 | 0.168579 |
| 26 | 90 | 21 | 21 | 1 | 0 | 26 | 164.0487 | 34.57021 | 28.78735 | 1.200882 | 0.306575 | 26 | 52.78415 | 73.99494 | 50.72693 | 1.458691 | 0.530027 |
| 27 | 90 | 21 | 21 | 1 | 0 | 27 | 3.30989 | 40.61481 | 25.67377 | 1.581957 | 0.600414 | 27 | 58.29538 | 65.38861 | 44.10026 | 1.482726 | 0.54514 |
| 28 | 90 | 21 | 21 | 1 | 0 | 28 | 173.3893 | 36.90399 | 32.28891 | 1.142931 | 0.234474 | 28 | 87.22237 | 71.72582 | 33.53174 | 2.139043 | 0.781445 |
| 29 | 90 | 21 | 21 | 1 | 0 | 29 | 128.1111 | 44.09251 | 24.72406 | 1.783385 | 0.68558 | 29 | 60.85293 | 55.65475 | 36.39412 | 1.529224 | 0.57238 |
| 30 | 90 | 21 | 21 | 1 | 0 | 30 | 158.3747 | 42.21863 | 22.25198 | 1.897298 | 0.722202 | 30 | 45.7722 | 45.43579 | 39.71704 | 1.143987 | 0.235887 |
| 31 | 90 | 21 | 21 | 1 | 0 | 31 | 142.0686 | 41.11554 | 22.08398 | 1.861781 | 0.711502 | 31 | 148.9243 | 49.39362 | 43.1312 | 1.145195 | 0.237497 |
| 32 | 90 | 21 | 21 | 1 | 0 | 32 | 47.83902 | 41.1167 | 27.07666 | 1.518529 | 0.566336 | 32 | 18.15495 | 47.52719 | 46.21878 | 1.028309 | 0.054302 |
| 33 | 90 | 21 | 21 | 1 | 0 | 33 | 129.5318 | 40.86987 | 25.48468 | 1.603703 | 0.611177 | 33 | 37.35847 | 48.54047 | 48.26935 | 1.005617 | 0.01114 |
| 34 | 90 | 21 | 21 | 1 | 0 | 34 | 128.4681 | 37.70828 | 23.94031 | 1.575096 | 0.596925 | 34 | 175.2604 | 43.95087 | 41.34006 | 1.063154 | 0.115277 |
| 35 | 90 | 21 | 21 | 1 | 0 | 35 | 140.4146 | 34.10962 | 25.70478 | 1.326976 | 0.432097 | 35 | 151.9683 | 45.71753 | 41.53911 | 1.10059 | 0.17444 |
| 36 | 90 | 21 | 21 | 1 | 0 | 36 | 125.7961 | 35.36652 | 25.10779 | 1.408588 | 0.495998 | 36 | 82.03367 | 47.84668 | 40.63144 | 1.177578 | 0.278858 |
| 37 | 90 | 21 | 21 | 1 | 0 | 37 | 39.52555 | 34.3643 | 25.33344 | 1.35648 | 0.456533 | 37 | 64.03983 | 45.26376 | 41.93848 | 1.079289 | 0.141532 |
| 38 | 90 | 21 | 21 | 1 | 0 | 38 | 18.26983 | 40.96265 | 21.81586 | 1.877655 | 0.716359 | 38 | 174.5741 | 49.51202 | 38.18031 | 1.296795 | 0.405355 |
| 39 | 90 | 21 | 21 | 1 | 0 | 39 | 53.73219 | 37.74707 | 24.50439 | 1.540421 | 0.578574 | 39 | 42.14469 | 47.49261 | 38.21295 | 1.242841 | 0.352605 |
| 40 | 90 | 21 | 21 | 1 | 0 | 40 | 5.85007 | 35.36719 | 27.32538 | 1.294298 | 0.403059 | 40 | 23.79506 | 41.40527 | 41.15549 | 1.006069 | 0.012029 |
| 41 | 90 | 21 | 21 | 1 | 0 | 41 | 119.2746 | 35.09839 | 23.70331 | 1.480738 | 0.543917 | 41 | 70.75026 | 71.12579 | 24.08392 | 2.953248 | 0.885343 |
| 42 | 90 | 21 | 21 | 1 | 0 | 42 | 121.1572 | 38.00842 | 24.0827 | 1.578246 | 0.598532 | 42 | 140.8504 | 47.08212 | 34.46213 | 1.366199 | 0.464238 |
| 43 | 90 | 21 | 21 | 1 | 0 | 43 | 106.9895 | 31.55203 | 24.38464 | 1.293931 | 0.40272 | 43 | 95.05094 | 54.11801 | 33.75896 | 1.603071 | 0.61087 |
| 44 | 90 | 21 | 21 | 1 | 0 | 44 | 170.2384 | 30.29196 | 26.20813 | 1.155823 | 0.251456 | 44 | 51.90938 | 45.57629 | 44.14996 | 1.032306 | 0.061611 |
| 45 | 90 | 21 | 21 | 1 | 0 | 45 | 178.6326 | 34.7868 | 22.92625 | 1.517335 | 0.565653 | 45 | 43.94479 | 59.08084 | 38.12906 | 1.549496 | 0.583496 |
| 46 | 90 | 21 | 21 | 1 | 0 | 46 | 90.38853 | 31.90491 | 22.79306 | 1.399764 | 0.489624 | 46 | 52.11748 | 53.80267 | 39.15356 | 1.374145 | 0.470416 |
| 47 | 90 | 21 | 21 | 1 | 0 | 47 | 47.80051 | 29.42792 | 25.68712 | 1.145629 | 0.238076 | 47 | 19.88452 | 42.05499 | 32.59045 | 1.290408 | 0.399455 |
| 48 | 180 | 21 | 19 | 1.105263 | 0.181406 | 48 | 133.3025 | 36.03748 | 17.85168 | 2.018716 | 0.754614 | 48 | 178.506 | 39.36648 | 39.17914 | 1.004782 | 0.009495 |
| 49 | 180 | 21 | 19 | 1.105263 | 0.181406 | 49 | 170.071 | 27.01971 | 24.01302 | 1.125211 | 0.210173 | 49 | 90.69621 | 40.82074 | 36.99945 | 1.10328 | 0.17846 |
| 50 | 90 | 21 | 19 | 1.105263 | 0.181406 | 50 | 113.0707 | 30.54202 | 24.96103 | 1.223588 | 0.332072 | 50 | 92.60884 | 47.97699 | 41.80762 | 1.147566 | 0.240645 |
| 51 | 180 | 21 | 19 | 1.105263 | 0.181406 | 51 | 149.5027 | 34.77965 | 20.64371 | 1.684758 | 0.64769 | 51 | 100.2121 | 47.16965 | 37.12048 | 1.270718 | 0.380699 |
| 52 | 180 | 21 | 19 | 1.105263 | 0.181406 | 52 | 28.17586 | 31.2254 | 22.06491 | 1.415161 | 0.500669 | 52 | 102.7738 | 43.30914 | 31.63086 | 1.369205 | 0.466588 |
| 53 | 180 | 21 | 19 | 1.105263 | 0.181406 | 53 | 58.52135 | 31.12744 | 22.06354 | 1.410809 | 0.497584 | 53 | 15.26862 | 39.66937 | 34.75952 | 1.141252 | 0.23222 |
| 54 | 90 | 21 | 19 | 1.105263 | 0.181406 | 54 | 121.0042 | 28.84711 | 20.73808 | 1.391021 | 0.483188 | 54 | 99.71647 | 49.11459 | 27.19019 | 1.806335 | 0.693519 |
| 55 | 180 | 21 | 19 | 1.105263 | 0.181406 | 55 | 78.58969 | 28.77379 | 23.01257 | 1.250351 | 0.360359 | 55 | 9.26252 | 36.05444 | 33.49344 | 1.076463 | 0.137017 |
| 56 | 180 | 21 | 19 | 1.105263 | 0.181406 | 56 | 33.43822 | 27.77856 | 22.99219 | 1.208174 | 0.31492 | 56 | 2.68695 | 48.85297 | 37.83066 | 1.291359 | 0.400339 |
| 57 | 90 | 21 | 19 | 1.105263 | 0.181406 | 57 | 129.8357 | 30.01188 | 21.60541 | 1.389091 | 0.481751 | 57 | 168.3995 | 47.00867 | 25.96164 | 1.810697 | 0.694994 |
| 58 | 90 | 21 | 19 | 1.105263 | 0.181406 | 58 | 16.58392 | 29.41595 | 20.78284 | 1.415396 | 0.500835 | 58 | 72.61831 | 55.30713 | 39.09613 | 1.414645 | 0.500305 |
| 59 | 90 | 21 | 19 | 1.105263 | 0.181406 | 59 | 143.2109 | 28.32477 | 19.97998 | 1.417658 | 0.502426 | 59 | 17.26376 | 38.73676 | 33.71826 | 1.148836 | 0.242324 |
| 60 | 180 | 21 | 19 | 1.105263 | 0.181406 | 60 | 148.8864 | 26.375 | 22.79016 | 1.157298 | 0.253362 | 60 | 6.9045 | 36.12372 | 31.91074 | 1.132024 | 0.219651 |
| 61 | 180 | 21 | 19 | 1.105263 | 0.181406 | 61 | 41.03456 | 25.67261 | 21.73682 | 1.181066 | 0.283111 | 61 | 86.89257 | 46.65771 | 24.90759 | 1.873233 | 0.715019 |
| 62 | 180 | 21 | 19 | 1.105263 | 0.181406 | 62 | 152.1994 | 31.39264 | 20.18785 | 1.555026 | 0.586453 | 62 | 42.79077 | 35.73334 | 28.66492 | 1.246588 | 0.356492 |
| 63 | 180 | 21 | 19 | 1.105263 | 0.181406 | 63 | 159.5077 | 34.80823 | 15.7805 | 2.205775 | 0.794469 | 63 | 26.26138 | 47.81459 | 26.96988 | 1.772888 | 0.681846 |
| 64 | 90 | 21 | 19 | 1.105263 | 0.181406 | 64 | 170.2187 | 25.12958 | 23.06224 | 1.089642 | 0.157766 | 64 | 103.7515 | 42.14136 | 31.43471 | 1.3406 | 0.443581 |
| 65 | 180 | 21 | 19 | 1.105263 | 0.181406 | 65 | 152.0996 | 41.12445 | 13.41328 | 3.06595 | 0.893618 | 65 | 34.97627 | 47.44757 | 26.47437 | 1.792208 | 0.688668 |
| 66 | 180 | 21 | 19 | 1.105263 | 0.181406 | 66 | 104.6625 | 31.25232 | 17.33408 | 1.802941 | 0.692364 | 66 | 71.50314 | 35.07794 | 31.7999 | 1.103083 | 0.178167 |
| 67 | 90 | 21 | 19 | 1.105263 | 0.181406 | 67 | 178.242 | 36.32611 | 17.70447 | 2.051804 | 0.762465 | 67 | 64.38512 | 37.64264 | 24.53192 | 1.534435 | 0.57528 |
| 68 | 180 | 21 | 19 | 1.105263 | 0.181406 | 68 | 111.8664 | 30.88062 | 21.67929 | 1.424429 | 0.507146 | 68 | 90.84727 | 42.29651 | 32.6405 | 1.295829 | 0.404469 |
| 69 | 180 | 21 | 19 | 1.105263 | 0.181406 | 69 | 120.7485 | 30.08057 | 17.96509 | 1.67439 | 0.643314 | 69 | 63.19698 | 50.49133 | 25.36548 | 1.990553 | 0.747621 |
| 70 | 90 | 21 | 19 | 1.105263 | 0.181406 | 70 | 92.41044 | 27.20206 | 16.39128 | 1.659545 | 0.636903 | 70 | 1.01415 | 56.85358 | 28.20873 | 2.01546 | 0.753821 |
| 71 | 90 | 19 | 19 | 1 | 0 | 71 | 107.5166 | 27.10895 | 18.93354 | 1.431795 | 0.512204 | 71 | 96.27859 | 34.42548 | 31.31636 | 1.099281 | 0.172472 |
| 72 | 90 | 19 | 19 | 1 | 0 | 72 | 139.8837 | 24.71625 | 21.27856 | 1.161557 | 0.258827 | 72 | 139.4407 | 36.55011 | 27.05398 | 1.351007 | 0.452121 |
| 73 | 90 | 19 | 19 | 1 | 0 | 73 | 69.59625 | 24.3573 | 22.1067 | 1.101806 | 0.176261 | 73 | 80.51788 | 40.30862 | 30.14548 | 1.337136 | 0.440695 |
| 74 | 90 | 19 | 19 | 1 | 0 | 74 | 12.93845 | 27.50323 | 18.01758 | 1.526466 | 0.570834 | 74 | 44.59735 | 37.00238 | 25.30162 | 1.462451 | 0.53244 |
| 75 | 90 | 19 | 19 | 1 | 0 | 75 | 48.752 | 23.91199 | 18.51648 | 1.29139 | 0.400367 | 75 | 125.6044 | 33.10406 | 26.82913 | 1.233885 | 0.343174 |
| 76 | 90 | 19 | 19 | 1 | 0 | 76 | 113.1076 | 27.61508 | 21.31696 | 1.295451 | 0.404121 | 76 | 107.3292 | 39.08447 | 36.98117 | 1.056875 | 0.104732 |
| 77 | 90 | 19 | 19 | 1 | 0 | 77 | 42.38636 | 25.32678 | 21.73125 | 1.165454 | 0.263777 | 77 | 58.21991 | 41.59238 | 21.90958 | 1.898365 | 0.722514 |
| 78 | 90 | 19 | 19 | 1 | 0 | 78 | 31.49225 | 24.74197 | 20.41583 | 1.211901 | 0.319128 | 78 | 24.19505 | 37.0473 | 26.17291 | 1.415483 | 0.500896 |
| 79 | 90 | 19 | 19 | 1 | 0 | 79 | 170.0638 | 24.552 | 19.84247 | 1.237346 | 0.346843 | 79 | 27.81589 | 33.12042 | 24.07477 | 1.375732 | 0.471637 |
| 80 | 90 | 19 | 19 | 1 | 0 | 80 | 35.69345 | 23.66492 | 19.29776 | 1.226304 | 0.335027 | 80 | 159.4036 | 31.56 | 25.37943 | 1.243527 | 0.35332 |
| 81 | 90 | 19 | 19 | 1 | 0 | 81 | 72.23466 | 25.1665 | 19.14377 | 1.314605 | 0.421359 | 81 | 177.6395 | 43.56567 | 19.73094 | 2.207988 | 0.794881 |
| 82 | 90 | 19 | 19 | 1 | 0 | 82 | 133.7856 | 28.78787 | 16.4502 | 1.750001 | 0.67347 | 82 | 151.8556 | 33.28784 | 21.33197 | 1.560467 | 0.589332 |
| 83 | 90 | 19 | 19 | 1 | 0 | 83 | 10.66128 | 26.97375 | 20.42979 | 1.320315 | 0.426352 | 83 | 89.4077 | 34.1684 | 21.28995 | 1.604907 | 0.61176 |
| 84 | 90 | 19 | 19 | 1 | 0 | 84 | 31.79601 | 24.03906 | 21.56116 | 1.114924 | 0.195531 | 84 | 110.8897 | 32.93036 | 30.12759 | 1.09303 | 0.16298 |
| 85 | 90 | 19 | 19 | 1 | 0 | 85 | 165.7826 | 22.74225 | 19.28241 | 1.17943 | 0.281121 | 85 | 118.4762 | 34.49258 | 22.30521 | 1.546391 | 0.581822 |
| 86 | 90 | 19 | 19 | 1 | 0 | 86 | 144.0112 | 24.08295 | 19.1693 | 1.256329 | 0.366432 | 86 | 129.3726 | 28.72668 | 24.07339 | 1.193296 | 0.297731 |
| 87 | 90 | 19 | 19 | 1 | 0 | 87 | 70.26888 | 22.67529 | 19.51391 | 1.162006 | 0.259401 | 87 | 67.49991 | 29.52859 | 25.0087 | 1.180733 | 0.282707 |
| 88 | 90 | 19 | 19 | 1 | 0 | 88 | 1.34867 | 26.92285 | 17.22913 | 1.562635 | 0.590471 | 88 | 89.68797 | 33.82422 | 20.00949 | 1.690409 | 0.650042 |
| 89 | 90 | 19 | 19 | 1 | 0 | 89 | 88.20458 | 22.50195 | 18.31164 | 1.228833 | 0.337762 | 89 | 17.80777 | 34.88794 | 22.51675 | 1.549422 | 0.583456 |
| 90 | 90 | 19 | 19 | 1 | 0 | 90 | 151.973 | 26.83673 | 16.48256 | 1.628189 | 0.622784 | 90 | 79.70654 | 29.4679 | 23.17233 | 1.271685 | 0.381641 |
| 91 | 90 | 19 | 19 | 1 | 0 | 91 | 47.55389 | 28.03931 | 14.23148 | 1.970231 | 0.742388 | 91 | 23.15711 | 28.06052 | 22.00922 | 1.274944 | 0.384798 |
| 92 | 90 | 19 | 19 | 1 | 0 | 92 | 29.88286 | 24.08221 | 17.33629 | 1.389121 | 0.481773 | 92 | 166.3697 | 26.43042 | 24.39044 | 1.083639 | 0.148409 |
| 93 | 90 | 19 | 19 | 1 | 0 | 93 | 2.96804 | 28.23376 | 15.00635 | 1.881454 | 0.717504 | 93 | 107.1958 | 32.01746 | 23.70406 | 1.350716 | 0.451885 |
| 94 | 90 | 19 | 19 | 1 | 0 | 94 | 149.9662 | 22.16385 | 18.24049 | 1.215091 | 0.322698 | 94 | 104.7084 | 26.6609 | 23.07306 | 1.155499 | 0.251036 |
| 95 | 90 | 19 | 19 | 1 | 0 | 95 | 130.7258 | 26.05023 | 15.51627 | 1.678898 | 0.645226 | 95 | 88.36651 | 34.76318 | 18.89877 | 1.839441 | 0.704452 |
| 96 | 90 | 19 | 19 | 1 | 0 | 96 | 158.7375 | 22.22939 | 17.18427 | 1.293589 | 0.402405 | 96 | 62.33725 | 29.01587 | 23.01056 | 1.260981 | 0.371098 |
| 97 | 90 | 19 | 19 | 1 | 0 | 97 | 174.1003 | 24.32178 | 17.81512 | 1.365232 | 0.463479 | 97 | 21.37976 | 31.62088 | 27.47211 | 1.151018 | 0.245193 |
| 98 | 90 | 19 | 19 | 1 | 0 | 98 | 144.2268 | 22.79532 | 20.37633 | 1.118716 | 0.200975 | 98 | 80.71279 | 24.23804 | 22.36069 | 1.083958 | 0.14891 |
| 99 | 90 | 19 | 19 | 1 | 0 | 99 | 28.42448 | 21.953 | 21.5397 | 1.019188 | 0.037299 | 99 | 125.5402 | 28.89008 | 24.03259 | 1.202121 | 0.308004 |
| 100 | 90 | 19 | 19 | 1 | 0 | 100 | 170.331 | 31.24695 | 17.11553 | 1.825649 | 0.699969 | 100 | 72.25814 | 29.80364 | 20.9675 | 1.421421 | 0.505058 |
| 101 | 178.5051 | 19.12396 | 17.12465 | 1.11675 | 0.19816 | 101 | 129.2939 | 22.88388 | 18.46937 | 1.239018 | 0.348604 | 101 | 100.0531 | 27.65741 | 18.01392 | 1.535335 | 0.575778 |
| 102 | 178.5051 | 19.12396 | 17.12463 | 1.116752 | 0.198162 | 102 | 41.89371 | 23.63181 | 15.09569 | 1.565467 | 0.591951 | 102 | 61.4824 | 28.40031 | 18.93353 | 1.500001 | 0.555556 |
| 103 | 178.5051 | 19.12396 | 17.12469 | 1.116748 | 0.198156 | 103 | 138.5616 | 22.52725 | 16.29852 | 1.382165 | 0.476544 | 103 | 65.54389 | 30.18732 | 18.22073 | 1.656757 | 0.63568 |
| 104 | 178.5051 | 19.12396 | 17.12469 | 1.116748 | 0.198156 | 104 | 111.3367 | 25.32971 | 19.06757 | 1.328418 | 0.43333 | 104 | 62.42252 | 32.47778 | 17.45689 | 1.860456 | 0.711091 |
| 105 | 178.5051 | 19.12396 | 17.12465 | 1.11675 | 0.19816 | 105 | 51.20837 | 21.56519 | 14.14334 | 1.524759 | 0.569872 | 105 | 149.0001 | 25.26477 | 20.24434 | 1.247992 | 0.357939 |
| 106 | 90 | 19 | 17 | 1.117647 | 0.199446 | 106 | 29.33712 | 21.26007 | 17.11349 | 1.242299 | 0.352041 | 106 | 125.4371 | 35.6709 | 13.81649 | 2.581763 | 0.849974 |
| 107 | 90 | 19 | 17 | 1.117647 | 0.199446 | 107 | 150.5022 | 25.62964 | 17.97424 | 1.42591 | 0.508169 | 107 | 78.12807 | 25.22571 | 22.31971 | 1.130199 | 0.217129 |
| 108 | 90 | 19 | 17 | 1.117647 | 0.199446 | 108 | 85.19893 | 19.82104 | 15.45038 | 1.282884 | 0.392389 | 108 | 87.94746 | 27.16299 | 17.67688 | 1.536639 | 0.576497 |
| 109 | 90 | 17 | 17 | 1 | 0 | 109 | 34.967 | 23.96985 | 14.38058 | 1.666821 | 0.640067 | 109 | 106.1202 | 30.23764 | 18.99467 | 1.591901 | 0.60539 |
| 110 | 90 | 17 | 17 | 1 | 0 | 110 | 62.4528 | 21.19739 | 15.63202 | 1.356024 | 0.456167 | 110 | 127.1258 | 26.01476 | 17.17218 | 1.514936 | 0.564276 |
| 111 | 90 | 17 | 17 | 1 | 0 | 111 | 121.8317 | 20.26462 | 18.60638 | 1.089122 | 0.156963 | 111 | 119.4336 | 25.49037 | 18.95129 | 1.345047 | 0.447254 |
| 112 | 90 | 17 | 17 | 1 | 0 | 112 | 41.51951 | 22.94019 | 15.40411 | 1.489225 | 0.549101 | 112 | 106.3239 | 21.89426 | 19.698 | 1.111497 | 0.190562 |
| 113 | 90 | 17 | 17 | 1 | 0 | 113 | 114.1257 | 21.93323 | 17.96257 | 1.221052 | 0.329295 | 113 | 105.6152 | 26.7525 | 23.83517 | 1.122396 | 0.206206 |
| 114 | 90 | 17 | 17 | 1 | 0 | 114 | 163.6127 | 19.48364 | 17.90137 | 1.088388 | 0.155825 | 114 | 85.82309 | 29.53583 | 14.66556 | 2.013959 | 0.753453 |
| 115 | 90 | 17 | 17 | 1 | 0 | 115 | 138.8325 | 19.67664 | 16.4481 | 1.196287 | 0.301237 | 115 | 118.1331 | 22.81378 | 20.60083 | 1.10742 | 0.184592 |
| 116 | 90 | 19 | 15 | 1.266667 | 0.376731 | 116 | 25.94465 | 24.66962 | 13.5946 | 1.814663 | 0.696326 | 116 | 91.15097 | 24.94812 | 16.7742 | 1.487291 | 0.547928 |
| 117 | 90 | 19 | 15 | 1.266667 | 0.376731 | 117 | 158.5195 | 21.83966 | 17.21194 | 1.268867 | 0.378891 | 117 | 62.4339 | 21.56262 | 19.34135 | 1.114846 | 0.195418 |
| 118 | 90 | 17 | 15 | 1.133333 | 0.221453 | 118 | 120.0836 | 24.36597 | 12.23029 | 1.992264 | 0.748055 | 118 | 13.49873 | 26.78815 | 14.56772 | 1.83887 | 0.704268 |
| 119 | 90 | 17 | 15 | 1.133333 | 0.221453 | 119 | 174.6803 | 22.40778 | 13.94998 | 1.606295 | 0.612431 | 119 | 172.5046 | 21.84119 | 15.20956 | 1.436017 | 0.515068 |
| 120 | 90 | 15 | 15 | 1 | 0 | 120 | 120.9573 | 27.12358 | 12.12726 | 2.236579 | 0.800091 | 120 | 132.3893 | 24.76703 | 19.96857 | 1.240301 | 0.349951 |
| 121 | 90 | 15 | 15 | 1 | 0 | 121 | 79.31702 | 22.81976 | 14.53088 | 1.570432 | 0.594527 | 121 | 44.81573 | 25.8479 | 11.86823 | 2.177907 | 0.789175 |
| 122 | 90 | 15 | 15 | 1 | 0 | 122 | 173.3637 | 18.38602 | 16.30194 | 1.127842 | 0.213854 | 122 | 109.0332 | 19.60504 | 16.80917 | 1.16633 | 0.264882 |
| 123 | 90 | 15 | 15 | 1 | 0 | 123 | 172.9556 | 22.63751 | 13.89073 | 1.629685 | 0.623476 | 123 | 4.78158 | 24.52631 | 13.45456 | 1.822899 | 0.699064 |
| 124 | 90 | 15 | 15 | 1 | 0 | 124 | 16.29719 | 23.71362 | 12.84848 | 1.845636 | 0.706433 | 124 | 136.3014 | 20.07629 | 18.11688 | 1.108154 | 0.185671 |
| 125 | 90 | 15 | 15 | 1 | 0 | 125 | 21.87079 | 18.8727 | 15.01508 | 1.256916 | 0.367024 | 125 | 127.3661 | 18.04207 | 15.34357 | 1.175872 | 0.276764 |
| 126 | 90 | 15 | 13 | 1.153846 | 0.248889 | 126 | 119.0316 | 21.08679 | 14.13959 | 1.49133 | 0.550373 | 126 | 162.7793 | 19.37018 | 15.01379 | 1.290159 | 0.399223 |