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Figure S1, S2, S3 and S4 show the schematic diagram of how the mortar is selected, the schematic diagram of how the basic grinding time is determined, the diagram of transmission electron microscope (TEM) characterization for gold and silver nanoparticles, and the schematic diagram of particle parameters as measured using the Image proplus 6.0 software, respectively. All raw data can be found as Table S1~6 .
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Figure S1. Schematic diagram of mortar selection. a, b) Particles produced in the glass mortar during grinding. c, d) Particles produced in an agate mortar during grinding.
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Figure S2. Image of the change occurring to plastic particles in the process of grinding. a~d) The corresponding grinding time is 0 min, 10 min, 20 min and 30 min, respectively.
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Figure S3. TEM characterization of gold and silver nanoparticles. a) Gold nanoparticles with a particle size of 40 nm. b) Silver nanoparticles with a particle size of 20 nm.
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Figure S4. Diagram of image processing by Image proplus 6.0 software processes image. a, e, h) Scanning electron microscope characteristic diagram of commercially available, self-made, and naturally-derived NPs. b~c, f~g, i~j) The software is used to select and measure the parameters of NPs.
Table S1. The number of NPs on the grinding conditions of different sample quality.

	
	1
	2
	3

	
	0.2g
	0.4g
	0.6g
	0.2g
	0.4g
	0.6g
	0.2g
	0.4g
	0.6g

	20 min
	5
	11
	25
	4
	12
	45
	6
	16
	53

	
	6
	15
	43
	8
	15
	35
	3
	14
	45

	
	8
	9
	46
	11
	25
	36
	2
	11
	49

	
	9
	16
	37
	3
	13
	40
	9
	10
	36

	
	8
	17
	32
	7
	19
	41
	8
	14
	29

	40 min
	4
	15
	35
	6
	19
	42
	9
	14
	30

	
	9
	22
	30
	9
	15
	34
	5
	13
	49

	
	8
	19
	19
	12
	21
	38
	1
	11
	38

	
	10
	18
	29
	0
	16
	36
	8
	19
	36

	
	12
	16
	37
	8
	13
	29
	6
	17
	32

	60 min
	8
	12
	16
	7
	19
	31
	6
	21
	43

	
	1
	16
	39
	3
	21
	36
	8
	13
	53

	
	6
	8
	46
	8
	23
	35
	2
	26
	46

	
	12
	16
	48
	6
	21
	50
	9
	10
	38

	
	7
	18
	42
	9
	15
	48
	11
	18
	34







	

2

Table S2. Dimension parameter of there kinds of NPs.
	Commercialized NP
	Self-made NPs
	Naturally-derived NPs

	Object
	Area
	Angle
	Size (length)
	Size (width)
	Object
	Area
	Angle
	Size (length)
	Size (width)
	Object
	Area
	Angle
	Size (length)
	Size (width)

	1
	1708
	128.4269
	65.2738
	33.45203
	1
	17585
	82.24453
	217.3941
	186.4578
	1
	19026
	36.73478
	211.8909
	180.4325

	2
	1323
	27.60772
	74.32281
	26.30844
	2
	17366
	27.06077
	186.1384
	186.061
	2
	3687
	175.7596
	84.10376
	57.80521

	3
	1090
	120.8743
	59.16776
	25.69424
	3
	16400
	134.8484
	200.769
	160.6791
	3
	1813
	89.92752
	55.00751
	48.01135

	4
	1068
	90
	37
	35
	4
	13970
	60.80544
	174.5122
	117.2835
	4
	1770
	51.12323
	67.97177
	47.68233

	5
	1016
	180
	35.00006
	35
	5
	7220
	29.69102
	135.4504
	82.51981
	5
	1426
	9.49547
	60.17126
	32.23199

	6
	1016
	180
	35
	35
	6
	6273
	113.963
	103.4639
	86.50756
	6
	1289
	76.8485
	65.34293
	30.57831

	7
	1016
	180
	35
	35
	7
	5232
	126.5374
	126.958
	76.95386
	7
	1266
	127.0528
	63.25586
	29.54495

	8
	1016
	180
	35
	35
	8
	5231
	142.616
	100.0857
	69.9523
	8
	1212
	117.2407
	47.81686
	39.33096

	9
	1016
	90
	35
	35
	9
	4490
	83.92727
	87.78128
	69.75525
	9
	1175
	179.2176
	54.09052
	31.90146

	10
	956
	90
	35
	33
	10
	4206
	130.3198
	116.4319
	66.86866
	10
	1146
	125.4936
	43.3587
	33.94877

	11
	905
	132.614
	33.41129
	32.85195
	11
	4017
	102.8392
	106.4246
	47.04959
	11
	1134
	133.7276
	55.36055
	28.27698

	12
	904
	90
	33
	33
	12
	3872
	122.2697
	94.65283
	68.75485
	12
	1086
	176.3997
	53.39777
	27.70023

	13
	904
	90
	33
	33
	13
	3859
	160.3207
	81.53949
	68.06934
	13
	1068
	74.6982
	44.72424
	39.46472

	14
	904
	90
	33
	33
	14
	3123
	52.42703
	74.56863
	64.021
	14
	1046
	4.04107
	46.22705
	34.49014

	15
	854
	1.82661
	33.20636
	31.20737
	15
	2979
	178.9376
	74.22833
	60.15659
	15
	1040
	117.6666
	61.29134
	22.61447

	16
	850
	90
	33
	31
	16
	2917
	78.62955
	68.63689
	61.77428
	16
	1031
	101.2473
	47.65765
	31.7811

	17
	804
	180
	31
	31
	17
	2581
	160.9083
	88.64755
	74.69009
	17
	1012
	66.29077
	55.65302
	26.50879

	18
	756
	27.82318
	42.57324
	21.54422
	18
	2497
	15.91475
	68.81534
	57.40659
	18
	990
	129.0647
	54.22849
	28.71759

	19
	751
	0.56423
	31.06743
	29.06752
	19
	2475
	23.30879
	64.85364
	50.79453
	19
	915
	61.56537
	55.28436
	29.31073

	20
	751
	0.56423
	31.06741
	29.06754
	20
	2433
	102.8152
	77.38788
	47.38191
	20
	909
	27.19413
	51.42648
	28.30042

	21
	704
	90
	29
	29
	21
	2260
	153.4441
	73.79276
	49.64342
	21
	901
	29.12935
	39.13531
	30.20001

	22
	602
	154.9549
	35.88318
	19.33833
	22
	2064
	29.59531
	55.60815
	52.72107
	22
	870
	13.64577
	54.54279
	23.73816

	23
	568
	90
	27
	25
	23
	2001
	71.86674
	67.32397
	41.52016
	23
	841
	88.59671
	44.13373
	30.89274

	24
	532
	180
	25
	25
	24
	1985
	149.6993
	70.11243
	54.06686
	24
	833
	21.02803
	50.83078
	25.91959

	25
	378
	90
	21
	21
	25
	1819
	7.31762
	57.07234
	52.03988
	25
	802
	173.4573
	42.55606
	29.49478

	26
	378
	90
	21
	21
	26
	1728
	145.0721
	73.99494
	50.72693
	26
	799
	38.32611
	34.57021
	28.78735

	27
	378
	90
	21
	21
	27
	1625
	43.92063
	65.38861
	44.10026
	27
	782
	16.7252
	40.61481
	25.67377

	28
	378
	90
	21
	21
	28
	1599
	16.3725
	71.72582
	33.53174
	28
	780
	132.8259
	36.90399
	32.28891

	29
	378
	90
	21
	21
	29
	1532
	17.02202
	55.65475
	36.39412
	29
	777
	164.0487
	44.09251
	24.72406

	30
	378
	90
	21
	21
	30
	1465
	128.0552
	45.43579
	39.71704
	30
	758
	3.30989
	42.21863
	22.25198

	31
	378
	90
	21
	21
	31
	1454
	39.30696
	49.39362
	43.1312
	31
	752
	173.3893
	41.11554
	22.08398

	32
	378
	90
	21
	21
	32
	1436
	173.9936
	47.52719
	46.21878
	32
	737
	128.1111
	41.1167
	27.07666

	33
	378
	90
	21
	21
	33
	1431
	9.10801
	48.54047
	48.26935
	33
	731
	158.3747
	40.86987
	25.48468

	34
	378
	90
	21
	21
	34
	1410
	52.78415
	43.95087
	41.34006
	34
	698
	142.0686
	37.70828
	23.94031

	35
	378
	90
	21
	21
	35
	1407
	58.29538
	45.71753
	41.53911
	35
	686
	47.83902
	34.10962
	25.70478

	36
	378
	90
	21
	21
	36
	1406
	87.22237
	47.84668
	40.63144
	36
	672
	129.5318
	35.36652
	25.10779

	37
	378
	90
	21
	21
	37
	1403
	60.85293
	45.26376
	41.93848
	37
	654
	128.4681
	34.3643
	25.33344

	38
	378
	90
	21
	21
	38
	1401
	45.7722
	49.51202
	38.18031
	38
	635
	140.4146
	40.96265
	21.81586

	39
	378
	90
	21
	21
	39
	1325
	148.9243
	47.49261
	38.21295
	39
	631
	125.7961
	37.74707
	24.50439

	40
	378
	90
	21
	21
	40
	1324
	18.15495
	41.40527
	41.15549
	40
	629
	39.52555
	35.36719
	27.32538

	41
	378
	90
	21
	21
	41
	1240
	37.35847
	71.12579
	24.08392
	41
	610
	18.26983
	35.09839
	23.70331

	42
	378
	90
	21
	21
	42
	1196
	175.2604
	47.08212
	34.46213
	42
	607
	53.73219
	38.00842
	24.0827

	43
	378
	90
	21
	21
	43
	1193
	151.9683
	54.11801
	33.75896
	43
	602
	5.85007
	31.55203
	24.38464

	44
	378
	90
	21
	21
	44
	1173
	82.03367
	45.57629
	44.14996
	44
	592
	119.2746
	30.29196
	26.20813

	45
	378
	90
	21
	21
	45
	1161
	64.03983
	59.08084
	38.12906
	45
	591
	121.1572
	34.7868
	22.92625

	46
	378
	90
	21
	21
	46
	1088
	174.5741
	53.80267
	39.15356
	46
	574
	106.9895
	31.90491
	22.79306

	47
	378
	90
	21
	21
	47
	1036
	42.14469
	42.05499
	32.59045
	47
	569
	170.2384
	29.42792
	25.68712

	48
	344
	180
	21
	19
	48
	1021
	23.79506
	39.36648
	39.17914
	48
	545
	178.6326
	36.03748
	17.85168

	49
	344
	180
	21
	19
	49
	1015
	70.75026
	40.82074
	36.99945
	49
	534
	90.38853
	27.01971
	24.01302

	50
	344
	90
	21
	19
	50
	1011
	140.8504
	47.97699
	41.80762
	50
	532
	47.80051
	30.54202
	24.96103

	51
	344
	180
	21
	19
	51
	919
	95.05094
	47.16965
	37.12048
	51
	532
	133.3025
	34.77965
	20.64371

	52
	344
	180
	21
	19
	52
	918
	51.90938
	43.30914
	31.63086
	52
	521
	170.071
	31.2254
	22.06491

	53
	344
	180
	21
	19
	53
	909
	43.94479
	39.66937
	34.75952
	53
	495
	113.0707
	31.12744
	22.06354

	54
	344
	90
	21
	19
	54
	905
	52.11748
	49.11459
	27.19019
	54
	477
	149.5027
	28.84711
	20.73808

	55
	344
	180
	21
	19
	55
	900
	19.88452
	36.05444
	33.49344
	55
	474
	28.17586
	28.77379
	23.01257

	56
	344
	180
	21
	19
	56
	884
	178.506
	48.85297
	37.83066
	56
	470
	58.52135
	27.77856
	22.99219

	57
	344
	90
	21
	19
	57
	874
	90.69621
	47.00867
	25.96164
	57
	467
	121.0042
	30.01188
	21.60541

	58
	344
	90
	21
	19
	58
	872
	92.60884
	55.30713
	39.09613
	58
	462
	78.58969
	29.41595
	20.78284

	59
	344
	90
	21
	19
	59
	869
	100.2121
	38.73676
	33.71826
	59
	460
	33.43822
	28.32477
	19.97998

	60
	344
	180
	21
	19
	60
	840
	102.7738
	36.12372
	31.91074
	60
	456
	129.8357
	26.375
	22.79016

	61
	344
	180
	21
	19
	61
	832
	15.26862
	46.65771
	24.90759
	61
	454
	16.58392
	25.67261
	21.73682

	62
	344
	180
	21
	19
	62
	796
	99.71647
	35.73334
	28.66492
	62
	451
	143.2109
	31.39264
	20.18785

	63
	344
	180
	21
	19
	63
	790
	9.26252
	47.81459
	26.96988
	63
	442
	148.8864
	34.80823
	15.7805

	64
	344
	90
	21
	19
	64
	789
	2.68695
	42.14136
	31.43471
	64
	433
	41.03456
	25.12958
	23.06224

	65
	344
	180
	21
	19
	65
	769
	168.3995
	47.44757
	26.47437
	65
	431
	152.1994
	41.12445
	13.41328

	66
	344
	180
	21
	19
	66
	768
	72.61831
	35.07794
	31.7999
	66
	430
	159.5077
	31.25232
	17.33408

	67
	344
	90
	21
	19
	67
	764
	17.26376
	37.64264
	24.53192
	67
	430
	170.2187
	36.32611
	17.70447

	68
	344
	180
	21
	19
	68
	745
	6.9045
	42.29651
	32.6405
	68
	424
	152.0996
	30.88062
	21.67929

	69
	344
	180
	21
	19
	69
	739
	86.89257
	50.49133
	25.36548
	69
	417
	104.6625
	30.08057
	17.96509

	70
	344
	90
	21
	19
	70
	731
	42.79077
	56.85358
	28.20873
	70
	406
	178.242
	27.20206
	16.39128

	71
	314
	90
	19
	19
	71
	722
	26.26138
	34.42548
	31.31636
	71
	406
	111.8664
	27.10895
	18.93354

	72
	314
	90
	19
	19
	72
	719
	103.7515
	36.55011
	27.05398
	72
	396
	120.7485
	24.71625
	21.27856

	73
	314
	90
	19
	19
	73
	716
	34.97627
	40.30862
	30.14548
	73
	392
	92.41044
	24.3573
	22.1067

	74
	314
	90
	19
	19
	74
	694
	71.50314
	37.00238
	25.30162
	74
	388
	107.5166
	27.50323
	18.01758

	75
	314
	90
	19
	19
	75
	685
	64.38512
	33.10406
	26.82913
	75
	377
	139.8837
	23.91199
	18.51648

	76
	314
	90
	19
	19
	76
	652
	90.84727
	39.08447
	36.98117
	76
	377
	69.59625
	27.61508
	21.31696

	77
	314
	90
	19
	19
	77
	609
	63.19698
	41.59238
	21.90958
	77
	376
	12.93845
	25.32678
	21.73125

	78
	314
	90
	19
	19
	78
	602
	1.01415
	37.0473
	26.17291
	78
	374
	48.752
	24.74197
	20.41583

	79
	314
	90
	19
	19
	79
	597
	96.27859
	33.12042
	24.07477
	79
	372
	113.1076
	24.552
	19.84247

	80
	314
	90
	19
	19
	80
	591
	139.4407
	31.56
	25.37943
	80
	372
	42.38636
	23.66492
	19.29776

	81
	314
	90
	19
	19
	81
	589
	80.51788
	43.56567
	19.73094
	81
	369
	31.49225
	25.1665
	19.14377

	82
	314
	90
	19
	19
	82
	579
	44.59735
	33.28784
	21.33197
	82
	368
	170.0638
	28.78787
	16.4502

	83
	314
	90
	19
	19
	83
	557
	125.6044
	34.1684
	21.28995
	83
	362
	35.69345
	26.97375
	20.42979

	84
	314
	90
	19
	19
	84
	533
	107.3292
	32.93036
	30.12759
	84
	357
	72.23466
	24.03906
	21.56116

	85
	314
	90
	19
	19
	85
	529
	58.21991
	34.49258
	22.30521
	85
	356
	133.7856
	22.74225
	19.28241

	86
	314
	90
	19
	19
	86
	523
	24.19505
	28.72668
	24.07339
	86
	350
	10.66128
	24.08295
	19.1693

	87
	314
	90
	19
	19
	87
	521
	27.81589
	29.52859
	25.0087
	87
	349
	31.79601
	22.67529
	19.51391

	88
	314
	90
	19
	19
	88
	510
	159.4036
	33.82422
	20.00949
	88
	346
	165.7826
	26.92285
	17.22913

	89
	314
	90
	19
	19
	89
	504
	177.6395
	34.88794
	22.51675
	89
	346
	144.0112
	22.50195
	18.31164

	90
	314
	90
	19
	19
	90
	503
	151.8556
	29.4679
	23.17233
	90
	344
	70.26888
	26.83673
	16.48256

	91
	314
	90
	19
	19
	91
	493
	89.4077
	28.06052
	22.00922
	91
	342
	1.34867
	28.03931
	14.23148

	92
	314
	90
	19
	19
	92
	487
	110.8897
	26.43042
	24.39044
	92
	342
	88.20458
	24.08221
	17.33629

	93
	314
	90
	19
	19
	93
	486
	118.4762
	32.01746
	23.70406
	93
	336
	151.973
	28.23376
	15.00635

	94
	314
	90
	19
	19
	94
	479
	129.3726
	26.6609
	23.07306
	94
	330
	47.55389
	22.16385
	18.24049

	95
	314
	90
	19
	19
	95
	452
	67.49991
	34.76318
	18.89877
	95
	323
	29.88286
	26.05023
	15.51627

	96
	314
	90
	19
	19
	96
	442
	89.68797
	29.01587
	23.01056
	96
	316
	2.96804
	22.22939
	17.18427

	97
	314
	90
	19
	19
	97
	437
	17.80777
	31.62088
	27.47211
	97
	308
	149.9662
	24.32178
	17.81512

	98
	314
	90
	19
	19
	98
	411
	79.70654
	24.23804
	22.36069
	98
	308
	130.7258
	22.79532
	20.37633

	99
	312
	90
	19
	19
	99
	400
	23.15711
	28.89008
	24.03259
	99
	302
	158.7375
	21.953
	21.5397

	100
	312
	90
	19
	19
	100
	399
	166.3697
	29.80364
	20.9675
	100
	300
	174.1003
	31.24695
	17.11553

	101
	285
	178.5051
	19.12396
	17.12465
	101
	387
	107.1958
	27.65741
	18.01392
	101
	300
	144.2268
	22.88388
	18.46937

	102
	285
	178.5051
	19.12396
	17.12463
	102
	381
	104.7084
	28.40031
	18.93353
	102
	288
	28.42448
	23.63181
	15.09569

	103
	285
	178.5051
	19.12396
	17.12469
	103
	380
	88.36651
	30.18732
	18.22073
	103
	287
	170.331
	22.52725
	16.29852

	104
	285
	178.5051
	19.12396
	17.12469
	104
	379
	62.33725
	32.47778
	17.45689
	104
	284
	129.2939
	25.32971
	19.06757

	105
	285
	178.5051
	19.12396
	17.12465
	105
	371
	21.37976
	25.26477
	20.24434
	105
	280
	41.89371
	21.56519
	14.14334

	106
	284
	90
	19
	17
	106
	371
	80.71279
	35.6709
	13.81649
	106
	276
	138.5616
	21.26007
	17.11349

	107
	284
	90
	19
	17
	107
	369
	125.5402
	25.22571
	22.31971
	107
	275
	111.3367
	25.62964
	17.97424

	108
	284
	90
	19
	17
	108
	357
	72.25814
	27.16299
	17.67688
	108
	273
	51.20837
	19.82104
	15.45038

	109
	256
	90
	17
	17
	109
	347
	100.0531
	30.23764
	18.99467
	109
	272
	29.33712
	23.96985
	14.38058

	110
	256
	90
	17
	17
	110
	342
	61.4824
	26.01476
	17.17218
	110
	271
	150.5022
	21.19739
	15.63202

	111
	256
	90
	17
	17
	111
	329
	65.54389
	25.49037
	18.95129
	111
	269
	85.19893
	20.26462
	18.60638

	112
	256
	90
	17
	17
	112
	327
	62.42252
	21.89426
	19.698
	112
	268
	34.967
	22.94019
	15.40411

	113
	256
	90
	17
	17
	113
	315
	149.0001
	26.7525
	23.83517
	113
	260
	62.4528
	21.93323
	17.96257

	114
	256
	90
	17
	17
	114
	313
	125.4371
	29.53583
	14.66556
	114
	259
	121.8317
	19.48364
	17.90137

	115
	256
	90
	17
	17
	115
	308
	78.12807
	22.81378
	20.60083
	115
	259
	41.51951
	19.67664
	16.4481

	116
	248
	90
	19
	15
	116
	293
	87.94746
	24.94812
	16.7742
	116
	256
	114.1257
	24.66962
	13.5946

	117
	248
	90
	19
	15
	117
	278
	106.1202
	21.56262
	19.34135
	117
	252
	163.6127
	21.83966
	17.21194

	118
	224
	90
	17
	15
	118
	274
	127.1258
	26.78815
	14.56772
	118
	250
	138.8325
	24.36597
	12.23029

	119
	224
	90
	17
	15
	119
	273
	119.4336
	21.84119
	15.20956
	119
	247
	25.94465
	22.40778
	13.94998

	120
	208
	90
	15
	15
	120
	263
	106.3239
	24.76703
	19.96857
	120
	246
	158.5195
	27.12358
	12.12726

	121
	208
	90
	15
	15
	121
	255
	105.6152
	25.8479
	11.86823
	121
	245
	120.0836
	22.81976
	14.53088

	122
	208
	90
	15
	15
	122
	254
	85.82309
	19.60504
	16.80917
	122
	243
	174.6803
	18.38602
	16.30194

	123
	208
	90
	15
	15
	123
	247
	118.1331
	24.52631
	13.45456
	123
	240
	120.9573
	22.63751
	13.89073

	124
	208
	90
	15
	15
	124
	244
	91.15097
	20.07629
	18.11688
	124
	239
	79.31702
	23.71362
	12.84848

	125
	208
	90
	15
	15
	125
	234
	62.4339
	18.04207
	15.34357
	125
	221
	173.3637
	18.8727
	15.01508

	126
	176
	90
	15
	13
	126
	232
	13.49873
	19.37018
	15.01379
	126
	219
	172.9556
	21.08679
	14.13959

	
	
	
	
	
	127
	222
	172.5046
	21.86414
	14.32382
	127
	211
	16.29719
	19.80231
	14.2793

	
	
	
	
	
	128
	194
	132.3893
	20.83911
	10.75664
	128
	211
	21.87079
	20.24011
	13.55441

	
	
	
	
	
	129
	192
	44.81573
	22.61816
	12.03213
	129
	205
	119.0316
	18.74632
	14.27832

	
	
	
	
	
	130
	187
	109.0332
	20.24408
	12.38837
	130
	199
	25.22953
	19.26666
	13.7869

	
	
	
	
	
	131
	180
	4.78158
	25.07971
	8.3056
	131
	196
	151.0249
	16.90387
	15.74693

	
	
	
	
	
	132
	164
	136.3014
	19.1673
	10.74841
	132
	193
	71.21966
	19.29529
	15.16724

	
	
	
	
	
	133
	160
	127.3661
	16.58899
	12.19604
	133
	190
	93.96064
	16.23807
	14.31192

	
	
	
	
	
	134
	154
	162.7793
	18.6734
	9.84776
	134
	180
	14.12861
	18.18781
	13.09494

	
	
	
	
	
	135
	144
	60.3303
	18.11511
	12.28561
	135
	144
	175.046
	17.19556
	9.87628

	
	
	
	
	
	136
	140
	127.4481
	15.6073
	12.3812
	136
	138
	133.5011
	14.1003
	13.44894

	
	
	
	
	
	137
	140
	100.7275
	13.51736
	12.53479
	137
	132
	121.9648
	15.05365
	11.13071

	
	
	
	
	
	138
	133
	59.53166
	18.70895
	9.68463
	138
	119
	168.0226
	13.96213
	10.6124

	
	
	
	
	
	139
	130
	116.0961
	13.87415
	12.53619
	
	
	
	
	

	
	
	
	
	
	140
	109
	72.68745
	14.55608
	8.76596
	
	
	
	
	



Table S3. Particle size distribution of there kinds of NPs with different particle sizes.
	80 nm Commercialized NPs
	50-100 nm Self-made NPs
	100-200 nm Self-made NPs
	200-400 nm Self-made NPs
	50-100 nm Naturally-derived NPs
	100-200 nm Naturally-derived NPs
	200-400 nm Naturally-derived NPs

	Size
	Intensity
	Size
	Intensity
	Size
	Intensity
	Size
	Intensity
	Size
	Intensity
	Size
	Intensity
	Size
	Intensity

	d.nm
	counts
	d.nm
	counts
	d.nm
	counts
	d.nm
	counts
	d.nm
	counts
	d.nm
	counts
	d.nm
	counts

	0.4
	0
	0.4
	0
	0.4
	0
	0.4
	0
	0.4
	0
	0.4
	0
	0.4
	0

	0.463
	0
	0.463
	0
	0.463
	0
	0.463
	0
	0.463
	0
	0.463
	0
	0.463
	0

	0.536
	0
	0.536
	0
	0.536
	0
	0.536
	0
	0.536
	0
	0.536
	0
	0.536
	0

	0.621
	0
	0.621
	0
	0.621
	0
	0.621
	0
	0.621
	0
	0.621
	0
	0.621
	0

	0.719
	0
	0.719
	0
	0.719
	0
	0.719
	0
	0.719
	0
	0.719
	0
	0.719
	0

	0.833
	0
	0.833
	0
	0.833
	0
	0.833
	0
	0.833
	0
	0.833
	0
	0.833
	0

	0.965
	0
	0.965
	0
	0.965
	0
	0.965
	0
	0.965
	0
	0.965
	0
	0.965
	0

	1.12
	0
	1.12
	0
	1.12
	0
	1.12
	0
	1.12
	0
	1.12
	0
	1.12
	0

	1.29
	0
	1.29
	0
	1.29
	0
	1.29
	0
	1.29
	0
	1.29
	0
	1.29
	0

	1.5
	0
	1.5
	0
	1.5
	0
	1.5
	0
	1.5
	0
	1.5
	0
	1.5
	0

	1.74
	0
	1.74
	0
	1.74
	0
	1.74
	0
	1.74
	0
	1.74
	0
	1.74
	0

	2.01
	0
	2.01
	0
	2.01
	0
	2.01
	0
	2.01
	0
	2.01
	0
	2.01
	0

	2.33
	0
	2.33
	0
	2.33
	0
	2.33
	0
	2.33
	0
	2.33
	0
	2.33
	0

	2.7
	0
	2.7
	0
	2.7
	0
	2.7
	0
	2.7
	0
	2.7
	0
	2.7
	0

	3.12
	0
	3.12
	0
	3.12
	0
	3.12
	0
	3.12
	0
	3.12
	0
	3.12
	0

	3.62
	0
	3.62
	0
	3.62
	0
	3.62
	0
	3.62
	0
	3.62
	0
	3.62
	0

	4.19
	0
	4.19
	0
	4.19
	0
	4.19
	0
	4.19
	0
	4.19
	0
	4.19
	0

	4.85
	0
	4.85
	0
	4.85
	0
	4.85
	0
	4.85
	0
	4.85
	0
	4.85
	0

	5.61
	0
	5.61
	0
	5.61
	0
	5.61
	0
	5.61
	0
	5.61
	0
	5.61
	0

	6.5
	0
	6.5
	0
	6.5
	0
	6.5
	0
	6.5
	0
	6.5
	0
	6.5
	0

	7.53
	0
	7.53
	0
	7.53
	0
	7.53
	0
	7.53
	0
	7.53
	0
	7.53
	0

	8.72
	0
	8.72
	0
	8.72
	0
	8.72
	0
	8.72
	0
	8.72
	0
	8.72
	0

	10.1
	0
	10.1
	0
	10.1
	0
	10.1
	0
	10.1
	0
	10.1
	0
	10.1
	0

	11.7
	0
	11.7
	0
	11.7
	0
	11.7
	0
	11.7
	0
	11.7
	0
	11.7
	0

	13.5
	0
	13.5
	0
	13.5
	0
	13.5
	0
	13.5
	0
	13.5
	0
	13.5
	0

	15.7
	0
	15.7
	0
	15.7
	0
	15.7
	0
	15.7
	0
	15.7
	0
	15.7
	0

	18.2
	0
	18.2
	0
	18.2
	0
	18.2
	0
	18.2
	0
	18.2
	0
	18.2
	0

	21
	0
	21
	0
	21
	0
	21
	0
	21
	0
	21
	0
	21
	0

	24.4
	0
	24.4
	0
	24.4
	0
	24.4
	0
	24.4
	0
	24.4
	0
	24.4
	0

	28.2
	0
	28.2
	0
	28.2
	0
	28.2
	0
	28.2
	0
	28.2
	0
	28.2
	0

	32.7
	0
	32.7
	0
	32.7
	0
	32.7
	0
	32.7
	0.0483
	32.7
	0
	32.7
	0

	37.8
	0
	37.8
	0
	37.8
	0
	37.8
	0
	37.8
	0.106
	37.8
	0
	37.8
	0

	43.8
	0
	43.8
	0
	43.8
	0.0895
	43.8
	0
	43.8
	0.122
	43.8
	0
	43.8
	0

	50.7
	1.21
	50.7
	0
	50.7
	0.986
	50.7
	0
	50.7
	0.188
	50.7
	0
	50.7
	0

	58.8
	6.48
	58.8
	0
	58.8
	3.15
	58.8
	0.0245
	58.8
	0.478
	58.8
	0.0139
	58.8
	0.0592

	68.1
	13.7
	68.1
	0
	68.1
	6.06
	68.1
	0.126
	68.1
	0.725
	68.1
	0.622
	68.1
	0.462

	78.8
	19.4
	78.8
	0
	78.8
	8.94
	78.8
	0.312
	78.8
	1.32
	78.8
	2.08
	78.8
	1.34

	91.3
	21.2
	91.3
	0
	91.3
	11.1
	91.3
	0.803
	91.3
	1.86
	91.3
	3.38
	91.3
	2.99

	106
	18.4
	106
	0.151
	106
	12.2
	106
	2.08
	106
	1.93
	106
	3.55
	106
	5.28

	122
	12.4
	122
	1.76
	122
	12.2
	122
	4.09
	122
	1.59
	122
	2.48
	122
	7.79

	142
	5.82
	142
	3.6
	142
	11.1
	142
	6.46
	142
	1.32
	142
	0.937
	142
	10

	164
	1.27
	164
	4.31
	164
	9.34
	164
	8.77
	164
	1.62
	164
	0
	164
	11.5

	190
	0
	190
	3.74
	190
	7.19
	190
	10.6
	190
	2.25
	190
	7.11
	190
	11.9

	220
	0
	220
	2.8
	220
	5.02
	220
	11.7
	220
	2.55
	220
	14.8
	220
	11.3

	255
	0
	255
	2.09
	255
	3.09
	255
	11.8
	255
	2.4
	255
	12.7
	255
	9.76

	295
	0
	295
	1.35
	295
	1.6
	295
	11
	295
	1.91
	295
	6.04
	295
	7.68

	342
	0
	342
	0.899
	342
	0.633
	342
	9.46
	342
	1.41
	342
	10.4
	342
	5.5

	396
	0
	396
	0.786
	396
	0.15
	396
	7.36
	396
	1.2
	396
	13.3
	396
	3.65

	459
	0
	459
	1.1
	459
	0.0249
	459
	5.06
	459
	3.46
	459
	12.3
	459
	2.34

	531
	0
	531
	2.16
	531
	0.0422
	531
	2.93
	531
	7.82
	531
	7.73
	531
	1.47

	615
	0
	615
	4.2
	615
	0.102
	615
	1.29
	615
	12
	615
	2.39
	615
	0.821

	712
	0
	712
	8.47
	712
	0.159
	712
	0.332
	712
	13.2
	712
	0
	712
	0.403

	825
	0
	825
	13
	825
	0.184
	825
	0.0317
	825
	10.6
	825
	0
	825
	0.158

	955
	0
	955
	15.3
	955
	0.168
	955
	0.0469
	955
	5.73
	955
	0
	955
	0.0254

	1110
	0
	1110
	13.7
	1110
	0.12
	1110
	0.108
	1110
	2.09
	1110
	0
	1110
	0

	1280
	0
	1280
	9.25
	1280
	0.0601
	1280
	0.155
	1280
	2.07
	1280
	0
	1280
	0

	1480
	0
	1480
	4.39
	1480
	0.0141
	1480
	0.173
	1480
	3.19
	1480
	0
	1480
	0

	1720
	0
	1720
	1.75
	1720
	3.04E-04
	1720
	0.164
	1720
	3.88
	1720
	0
	1720
	0

	1990
	0
	1990
	0.764
	1990
	0.0198
	1990
	0.142
	1990
	3.86
	1990
	0
	1990
	0

	2300
	0
	2300
	0.239
	2300
	0.0668
	2300
	0.129
	2300
	3.12
	2300
	0
	2300
	0

	2670
	0
	2670
	0
	2670
	0.161
	2670
	0.148
	2670
	1.94
	2670
	0
	2670
	0

	3090
	0
	3090
	0
	3090
	0.384
	3090
	0.219
	3090
	0.741
	3090
	0
	3090
	0

	3580
	0
	3580
	0
	3580
	0.747
	3580
	0.343
	3580
	0
	3580
	0
	3580
	0.0705

	4150
	0
	4150
	0.088
	4150
	1.2
	4150
	0.654
	4150
	0
	4150
	0
	4150
	0.371

	4800
	0
	4800
	0.787
	4800
	1.65
	4800
	1.32
	4800
	0.877
	4800
	0
	4800
	1.57

	5560
	0
	5560
	3.29
	5560
	1.98
	5560
	2.17
	5560
	2.47
	5560
	0
	5560
	3.51

	6440
	0
	6440
	0
	6440
	0
	6440
	0
	6440
	0
	6440
	0
	6440
	0

	7460
	0
	7460
	0
	7460
	0
	7460
	0
	7460
	0
	7460
	0
	7460
	0

	8630
	0
	8630
	0
	8630
	0
	8630
	0
	8630
	0
	8630
	0
	8630
	0



Table S4. Zeta potential of there kinds of NPs with different particle sizes.
	Groups
	Zeta potential

	Control
	-3.42
	-1.79
	-3.52

	80 nm PS NPs
	-43.5
	-45.8
	-45.6

	50~100 nm Self-made NPs
	-30.5
	-25.9
	-24.8

	100~200 nm Self-made NPs
	-30.5
	-31.1
	-30.5

	200~400 nm Self-made NPs
	-24
	-28.7
	-27.7

	50-100 nm Naturally-derived NPs
	-33.7
	-33.3
	-41.7

	100-200 nm Naturally-derived NPs
	-20.4
	-21.3
	-22.6

	200-400 nm Naturally-derived NPs
	-47.3
	-43.8
	-41




Table S5. Raman spectrum information of the three kinds of NPs.
	Raman shift
	Intensity
	Raman shift
	Intensity
	Raman shift
	Intensity
	Raman shift
	Intensity
	Raman shift
	Intensity
	Raman shift
	Intensity
	Raman shift
	Intensity
	Raman shift
	Intensity

	control
	PS NPs
	50-100 nm PP NPs
	100-200 nm PP NPs
	200-400 nm PP NPs
	50-100 nmNaturally-derived NPs
	100-200 nmNaturally-derived NPs
	200-400 nmNaturally-derived NPs

	600.181
	0
	600.502
	36.00755
	600.284
	0
	600.284
	0
	600.284
	0
	600.284
	0
	600.284
	0
	600.284
	0

	600.916
	1.36254
	601.238
	36.74855
	601.022
	61.7345
	601.022
	3.02767
	601.022
	27.7032
	601.022
	2.67972
	601.022
	27.23013
	601.022
	62.01522

	601.652
	2.71405
	601.975
	35.02755
	601.76
	62.73638
	601.76
	23.09208
	601.76
	50.81838
	601.76
	22.39618
	601.76
	49.87223
	601.76
	63.29783

	602.389
	4.00495
	602.713
	35.18018
	602.496
	73.36806
	602.496
	41.00991
	602.496
	52.21485
	602.496
	39.967
	602.496
	50.79692
	602.496
	74.20947

	603.125
	5.25879
	603.449
	34.963
	603.233
	76.92268
	603.233
	53.27456
	603.233
	56.38089
	603.233
	51.88418
	603.233
	54.49053
	603.233
	78.04442

	603.861
	6.49062
	604.186
	35.56482
	603.971
	85.56363
	603.971
	56.8922
	603.971
	68.89685
	603.971
	55.15387
	603.971
	66.53342
	603.971
	86.96609

	604.597
	7.69585
	604.924
	35.305
	604.708
	91.14075
	604.708
	61.5163
	604.708
	76.29546
	604.708
	59.43049
	604.708
	73.45959
	604.708
	92.82356

	605.333
	8.8428
	605.66
	35.00964
	605.445
	92.08564
	605.445
	69.31533
	605.445
	81.51836
	605.445
	66.88204
	605.445
	78.21006
	605.445
	94.04879

	606.068
	9.93406
	606.397
	34.77036
	606.182
	96.64043
	606.182
	74.65956
	606.182
	84.88243
	606.182
	71.87879
	606.182
	81.1017
	606.182
	98.88392

	606.804
	10.95935
	607.134
	32.77655
	606.92
	102.7032
	606.92
	77.58677
	606.92
	87.75162
	606.92
	74.45805
	606.92
	83.49781
	606.92
	105.2274

	607.54
	11.90381
	607.869
	32.61118
	607.657
	104.1954
	607.657
	83.22178
	607.657
	92.0426
	607.657
	79.74559
	607.657
	87.31637
	607.657
	106.9999

	608.275
	12.77463
	608.606
	33.30673
	608.392
	108.853
	608.392
	87.0017
	608.392
	97.64133
	608.392
	83.17897
	608.392
	92.44394
	608.392
	111.9372

	609.011
	13.57484
	609.342
	34.29227
	609.129
	111.8133
	609.129
	91.22565
	609.129
	103.594
	609.129
	87.05545
	609.129
	97.92413
	609.129
	115.1778

	609.746
	14.30355
	610.079
	36.09855
	609.866
	113.7567
	609.866
	92.00876
	609.866
	109.5968
	609.866
	87.49107
	609.866
	103.4546
	609.866
	117.4015

	610.482
	14.97256
	610.815
	36.60891
	610.603
	115.1617
	610.603
	94.37663
	610.603
	114.126
	610.603
	89.51147
	610.603
	107.5113
	610.603
	119.0868

	611.215
	15.59103
	611.551
	37.31982
	611.339
	118.0356
	611.339
	99.60324
	611.339
	119.9372
	611.339
	94.39107
	611.339
	112.8507
	611.339
	122.2408

	611.951
	16.1677
	612.287
	39.98618
	612.076
	118.5561
	612.076
	103.8013
	612.076
	123.222
	612.076
	98.24166
	612.076
	115.6631
	612.076
	123.0416

	612.686
	16.70471
	613.024
	41.22055
	612.813
	120.8059
	612.813
	108.1927
	612.813
	126.9709
	612.813
	102.2856
	612.813
	118.9396
	612.813
	125.5717

	613.421
	17.19857
	613.759
	40.81745
	613.548
	122.8866
	613.548
	109.341
	613.548
	129.1156
	613.548
	103.0873
	613.548
	120.6131
	613.548
	127.932

	614.156
	17.65235
	614.495
	41.61018
	614.284
	125.564
	614.284
	111.6626
	614.284
	131.0636
	614.284
	105.0619
	614.284
	122.0893
	614.284
	130.8894

	614.891
	18.06539
	615.23
	41.26882
	615.02
	129.49
	615.02
	115.0905
	615.02
	135.833
	615.02
	108.1429
	615.02
	126.3869
	615.02
	135.0953

	615.626
	18.44914
	615.966
	41.72009
	615.757
	133.1925
	615.757
	117.792
	615.757
	139.0796
	615.757
	110.4968
	615.757
	129.1611
	615.757
	139.0782

	616.361
	18.81112
	616.703
	41.92236
	616.493
	136.2601
	616.493
	122.4338
	616.493
	144.3402
	616.493
	114.7916
	616.493
	133.9499
	616.493
	142.4257

	617.095
	19.16301
	617.437
	41.52591
	617.229
	140.3259
	617.229
	127.1233
	617.229
	146.9062
	617.229
	119.1341
	617.229
	136.0442
	617.229
	146.7715

	617.83
	19.52094
	618.173
	40.75673
	617.964
	144.2318
	617.964
	130.7988
	617.964
	151.6394
	617.964
	122.4631
	617.964
	140.3062
	617.964
	150.9569

	618.563
	19.8962
	618.908
	39.62991
	618.7
	147.6753
	618.7
	135.3208
	618.7
	156.6966
	618.7
	126.6381
	618.7
	144.8916
	618.7
	154.6804

	619.298
	20.28745
	619.644
	40.35227
	619.435
	152.665
	619.435
	139.8945
	619.435
	162.2962
	619.435
	130.8652
	619.435
	150.0201
	619.435
	159.9497

	620.032
	20.69442
	620.38
	39.92018
	620.171
	155.9595
	620.171
	145.8641
	620.171
	167.5925
	620.171
	136.4878
	620.171
	154.8446
	620.171
	163.5242

	620.766
	21.11364
	621.114
	38.74927
	620.907
	158.7992
	620.907
	150.6601
	620.907
	172.3789
	620.907
	140.9368
	620.907
	159.1592
	620.907
	166.6438

	621.501
	21.53592
	621.85
	38.66073
	621.641
	162.4847
	621.641
	154.4896
	621.641
	175.9984
	621.641
	144.4203
	621.641
	162.3081
	621.641
	170.6085

	622.235
	21.95657
	622.584
	38.18227
	622.377
	166.7111
	622.377
	159.3232
	622.377
	179.2851
	622.377
	148.9068
	622.377
	165.1231
	622.377
	175.1148

	622.969
	22.37161
	623.319
	38.00745
	623.113
	169.5303
	623.113
	162.2124
	623.113
	184.5292
	623.113
	151.4491
	623.113
	169.8954
	623.113
	178.214

	623.702
	22.78231
	624.053
	37.44082
	623.848
	171.9236
	623.848
	165.5256
	623.848
	189.9965
	623.848
	154.4158
	623.848
	174.8916
	623.848
	180.8869

	624.436
	23.19102
	624.789
	35.99836
	624.583
	174.2077
	624.583
	168.3418
	624.583
	194.6022
	624.583
	156.8854
	624.583
	179.0261
	624.583
	183.4506

	625.17
	23.60113
	625.523
	35.75782
	625.317
	176.2782
	625.317
	170.5164
	625.317
	199.0298
	625.317
	158.714
	625.317
	182.9832
	625.317
	185.8003

	625.904
	24.01108
	626.258
	35.45464
	626.053
	177.9003
	626.053
	173.4961
	626.053
	202.0008
	626.053
	161.3467
	626.053
	185.4824
	626.053
	187.7023

	626.637
	24.41605
	626.993
	35.15618
	626.788
	179.4524
	626.788
	177.0329
	626.788
	204.7064
	626.788
	164.5369
	626.788
	187.7168
	626.788
	189.534

	627.371
	24.81237
	627.727
	33.23482
	627.523
	180.3983
	627.523
	178.7491
	627.523
	207.9644
	627.523
	165.9066
	627.523
	190.5037
	627.523
	190.7595

	628.103
	25.1987
	628.462
	33.23573
	628.258
	182.0732
	628.258
	181.1884
	628.258
	210.6027
	628.258
	167.9993
	628.258
	192.6708
	628.258
	192.714

	628.837
	25.57176
	629.195
	35.199
	628.992
	184.3097
	628.992
	182.7802
	628.992
	213.4345
	628.992
	169.2451
	628.992
	195.0321
	628.992
	195.2297

	629.571
	25.93087
	629.93
	36.04973
	629.727
	185.5956
	629.727
	183.8234
	629.727
	215.8773
	629.727
	169.9417
	629.727
	197.0038
	629.727
	196.7951

	630.304
	26.27423
	630.664
	36.54473
	630.461
	186.0702
	630.461
	185.8489
	630.461
	217.9904
	630.461
	171.6212
	630.461
	198.6464
	630.461
	197.5489

	631.037
	26.5969
	631.398
	37.85109
	631.196
	187.191
	631.196
	187.544
	631.196
	220.4485
	631.196
	172.9697
	631.196
	200.6333
	631.196
	198.9493

	631.769
	26.89226
	632.132
	38.56045
	631.929
	188.1628
	631.929
	188.7633
	631.929
	223.7821
	631.929
	173.8435
	631.929
	203.4971
	631.929
	200.2

	632.503
	27.15765
	632.866
	38.24882
	632.664
	188.9373
	632.664
	190.0426
	632.664
	227.4696
	632.664
	174.7762
	632.664
	206.7134
	632.664
	201.2541

	633.236
	27.39423
	633.599
	38.87764
	633.399
	190.2076
	633.399
	191.1474
	633.399
	230.2435
	633.399
	175.5345
	633.399
	209.0161
	633.399
	202.804

	633.969
	27.60334
	634.334
	39.37464
	634.133
	190.8412
	634.133
	191.6208
	634.133
	231.8662
	634.133
	175.6618
	634.133
	210.1684
	634.133
	203.7167

	634.702
	27.78763
	635.067
	40.17418
	634.866
	190.4519
	634.866
	192.6925
	634.866
	234.2918
	634.866
	176.3879
	634.866
	212.1241
	634.866
	203.6062

	635.433
	27.95007
	635.801
	41.87818
	635.6
	190.6176
	635.6
	193.784
	635.6
	235.541
	635.6
	177.1334
	635.6
	212.9028
	635.6
	204.0511

	636.166
	28.08977
	636.534
	41.70409
	636.335
	189.5581
	636.335
	193.1504
	636.335
	236.8622
	636.335
	176.1532
	636.335
	213.7528
	636.335
	203.2713

	636.899
	28.20714
	637.268
	40.23382
	637.069
	188.9405
	637.069
	193.9944
	637.069
	237.6485
	637.069
	176.6511
	637.069
	214.0686
	637.069
	202.9329

	637.632
	28.30322
	638.001
	39.89655
	637.802
	187.944
	637.802
	194.7222
	637.802
	239.2089
	637.802
	177.0333
	637.802
	215.1592
	637.802
	202.2151

	638.364
	28.37504
	638.735
	39.82591
	638.536
	188.5397
	638.536
	195.7094
	638.536
	239.503
	638.536
	177.6745
	638.536
	214.9828
	638.536
	203.0901

	639.096
	28.42299
	639.468
	40.43009
	639.27
	188.6742
	639.27
	196.5159
	639.27
	239.2226
	639.27
	178.1349
	639.27
	214.2318
	639.27
	203.5037

	639.828
	28.44999
	640.201
	41.002
	640.004
	188.3754
	640.004
	196.697
	640.004
	239.2708
	640.004
	177.97
	640.004
	213.8096
	640.004
	203.4842

	640.561
	28.45654
	640.934
	41.00255
	640.736
	188.0781
	640.736
	195.7755
	640.736
	239.0518
	640.736
	176.7034
	640.736
	213.1213
	640.736
	203.4653

	641.293
	28.44131
	641.668
	40.56809
	641.47
	186.9552
	641.47
	196.0652
	641.47
	238.5316
	641.47
	176.6469
	641.47
	212.1306
	641.47
	202.6216

	642.024
	28.3995
	642.4
	41.23091
	642.203
	187.3436
	642.203
	195.7855
	642.203
	239.1734
	642.203
	176.0217
	642.203
	212.3026
	642.203
	203.2888

	642.756
	28.33111
	643.133
	41.77355
	642.936
	186.4451
	642.936
	196.0746
	642.936
	239.0569
	642.936
	175.9652
	642.936
	211.7162
	642.936
	202.6691

	643.488
	28.23841
	643.866
	42.19336
	643.669
	185.9096
	643.669
	195.4025
	643.669
	239.4298
	643.669
	174.9475
	643.669
	211.6191
	643.669
	202.4125

	644.22
	28.12257
	644.599
	41.32809
	644.403
	184.8476
	644.403
	194.641
	644.403
	238.6666
	644.403
	173.84
	644.403
	210.3855
	644.403
	201.6296

	644.951
	27.9874
	645.331
	41.91218
	645.136
	183.6858
	645.136
	194.4829
	645.136
	239.7126
	645.136
	173.3363
	645.136
	210.9616
	645.136
	200.7467

	645.683
	27.83269
	646.064
	41.07027
	645.868
	183.4104
	645.868
	195.4573
	645.868
	240.6127
	645.868
	173.9655
	645.868
	211.3925
	645.868
	200.7497

	646.415
	27.65483
	646.796
	41.25255
	646.601
	182.0092
	646.601
	194.0964
	646.601
	241.9204
	646.601
	172.259
	646.601
	212.2303
	646.601
	199.6274

	647.147
	27.45547
	647.529
	40.10273
	647.335
	180.1551
	647.335
	193.5185
	647.335
	242.7307
	647.335
	171.3351
	647.335
	212.5701
	647.335
	198.0524

	647.877
	27.2379
	648.261
	38.65355
	648.066
	178.4659
	648.066
	192.9386
	648.066
	242.5977
	648.066
	170.4105
	648.066
	211.9685
	648.066
	196.6413

	648.609
	27.00464
	648.994
	38.95136
	648.799
	175.7849
	648.799
	193.2495
	648.799
	242.7848
	648.799
	170.3759
	648.799
	211.6857
	648.799
	194.2391

	649.34
	26.75804
	649.726
	39.14473
	649.532
	173.221
	649.532
	192.5173
	649.532
	244.2321
	649.532
	169.298
	649.532
	212.6632
	649.532
	191.954

	650.072
	26.5006
	650.457
	38.85182
	650.264
	172.1131
	650.264
	191.7744
	650.264
	243.7301
	650.264
	168.21
	650.264
	211.6919
	650.264
	191.1246

	650.802
	26.23434
	651.19
	39.50336
	650.997
	170.4698
	650.997
	189.0944
	650.997
	243.0091
	650.997
	165.1844
	650.997
	210.5012
	650.997
	189.7601

	651.533
	25.96436
	651.922
	37.30518
	651.73
	168.5394
	651.73
	187.4974
	651.73
	241.5089
	651.73
	163.2418
	651.73
	208.5311
	651.73
	188.1085

	652.265
	25.69486
	652.654
	36.92836
	652.461
	165.8044
	652.461
	184.7568
	652.461
	240.6032
	652.461
	160.1566
	652.461
	207.1568
	652.461
	185.6515

	652.995
	25.42894
	653.385
	36.84818
	653.194
	163.4245
	653.194
	183.5455
	653.194
	242.3671
	653.194
	158.5997
	653.194
	208.4508
	653.194
	183.5505

	653.726
	25.17126
	654.118
	37.49455
	653.926
	161.0609
	653.926
	182.6602
	653.926
	241.2489
	653.926
	157.3693
	653.926
	206.8634
	653.926
	181.4653

	654.457
	24.92834
	654.849
	36.94045
	654.657
	158.4391
	654.657
	180.5624
	654.657
	240.0919
	654.657
	154.9269
	654.657
	205.2378
	654.657
	179.1216

	655.188
	24.70243
	655.581
	37.09964
	655.39
	156.0923
	655.39
	178.0017
	655.39
	239.4514
	655.39
	152.0205
	655.39
	204.1275
	655.39
	177.0537

	655.918
	24.49279
	656.312
	39.387
	656.122
	154.401
	656.122
	174.9798
	656.122
	237.4065
	656.122
	148.6535
	656.122
	201.6133
	656.122
	175.6407

	656.648
	24.29712
	657.043
	40.11664
	656.853
	151.5834
	656.853
	172.8908
	656.853
	235.8545
	656.853
	146.2199
	656.853
	199.5927
	656.853
	173.1012

	657.379
	24.11269
	657.775
	39.56345
	657.585
	148.899
	657.585
	170.4175
	657.585
	234.3917
	657.585
	143.4014
	657.585
	197.6607
	657.585
	170.6952

	658.109
	23.94175
	658.506
	39.53836
	658.317
	146.4773
	658.317
	166.6813
	658.317
	232.3865
	658.317
	139.3202
	658.317
	195.1862
	658.317
	168.552

	658.839
	23.78497
	659.238
	38.21591
	659.048
	143.5226
	659.048
	163.3622
	659.048
	230.9122
	659.048
	135.6564
	659.048
	193.2434
	659.048
	165.8754

	659.57
	23.6413
	659.969
	39.61555
	659.78
	139.4649
	659.78
	160.0809
	659.78
	230.856
	659.78
	132.0299
	659.78
	192.7179
	659.78
	162.0961

	660.299
	23.51018
	660.699
	39.67273
	660.512
	136.8687
	660.512
	157.9348
	660.512
	227.4591
	660.512
	129.5388
	660.512
	188.8518
	660.512
	159.7783

	661.03
	23.38964
	661.431
	38.11364
	661.242
	134.3176
	661.242
	155.9788
	661.242
	224.3709
	661.242
	127.2385
	661.242
	185.2957
	661.242
	157.5049

	661.76
	23.28118
	662.162
	38.598
	661.974
	132.879
	661.974
	154.7455
	661.974
	222.8256
	661.974
	125.6602
	661.974
	183.2811
	661.974
	156.3447

	662.489
	23.1853
	662.893
	38.70018
	662.704
	130.2254
	662.704
	152.6002
	662.704
	220.5326
	662.704
	123.1707
	662.704
	180.5202
	662.704
	153.9688

	663.219
	23.0983
	663.623
	38.46318
	663.436
	127.0182
	663.436
	150.2168
	663.436
	218.4031
	663.436
	120.4421
	663.436
	177.9215
	663.436
	151.0401

	663.949
	23.01861
	664.354
	38.09391
	664.168
	124.7088
	664.168
	147.2817
	664.168
	216.9757
	664.168
	117.1619
	664.168
	176.0248
	664.168
	149.0091

	664.678
	22.94438
	665.085
	37.58073
	664.898
	122.1206
	664.898
	145.4974
	664.898
	214.7697
	664.898
	115.0335
	664.898
	173.3509
	664.898
	146.6986

	665.408
	22.87226
	665.815
	37.00018
	665.629
	119.1467
	665.629
	143.4035
	665.629
	212.9294
	665.629
	112.5949
	665.629
	171.042
	665.629
	144.0027

	666.138
	22.79855
	666.545
	38.11136
	666.359
	116.063
	666.359
	140.7427
	666.359
	211.5495
	666.359
	109.5899
	666.359
	169.1941
	666.359
	141.1967

	666.867
	22.72231
	667.276
	38.63455
	667.09
	113.7789
	667.09
	139.0921
	667.09
	210.9422
	667.09
	107.5946
	667.09
	168.1183
	667.09
	139.1906

	667.597
	22.64086
	668.006
	38.26318
	667.822
	112.5287
	667.822
	135.8528
	667.822
	210.2089
	667.822
	104.0103
	667.822
	166.9158
	667.822
	138.2189

	668.325
	22.55259
	668.737
	39.24355
	668.551
	109.742
	668.551
	132.8792
	668.551
	209.5341
	668.551
	100.693
	668.551
	165.7737
	668.551
	135.7096

	669.055
	22.45569
	669.467
	41.45391
	669.282
	107.2274
	669.282
	131.2861
	669.282
	207.756
	669.282
	98.75522
	669.282
	163.5269
	669.282
	133.473

	669.784
	22.34923
	670.197
	39.145
	670.012
	103.5716
	670.012
	129.6421
	670.012
	205.2955
	670.012
	96.76707
	670.012
	160.5985
	670.012
	130.0948

	670.512
	22.23066
	670.928
	38.10327
	670.743
	100.0015
	670.743
	127.1076
	670.743
	202.7887
	670.743
	93.88791
	670.743
	157.6232
	670.743
	126.8028

	671.242
	22.09609
	671.657
	37.35964
	671.474
	96.99366
	671.474
	125.6229
	671.474
	201.653
	671.474
	92.05848
	671.474
	156.0189
	671.474
	124.073

	671.971
	21.94299
	672.386
	35.28982
	672.203
	94.46278
	672.203
	123.0216
	672.203
	200.0307
	672.203
	89.11352
	672.203
	153.9292
	672.203
	121.8194

	672.699
	21.77113
	673.117
	35.69909
	672.934
	91.5236
	672.934
	120.8071
	672.934
	198.4489
	672.934
	86.55442
	672.934
	151.8789
	672.934
	119.1583

	673.429
	21.58133
	673.846
	36.61382
	673.663
	90.15877
	673.663
	120.1746
	673.663
	195.3688
	673.663
	85.57814
	673.663
	148.3315
	673.663
	118.0708

	674.156
	21.37378
	674.576
	35.43382
	674.394
	87.76393
	674.394
	118.5734
	674.394
	194.0663
	674.394
	83.6323
	674.394
	146.5604
	674.394
	115.954

	674.886
	21.15329
	675.306
	34.82827
	675.123
	86.31111
	675.123
	117.0196
	675.123
	191.9027
	675.123
	81.73481
	675.123
	143.9295
	675.123
	114.7785

	675.615
	20.91984
	676.035
	35.05627
	675.853
	83.4288
	675.853
	115.6655
	675.853
	190.6499
	675.853
	80.03651
	675.853
	142.2088
	675.853
	112.1739

	676.342
	20.67337
	676.764
	33.50282
	676.584
	80.57246
	676.584
	114.2743
	676.584
	190.578
	676.584
	78.30068
	676.584
	141.6683
	676.584
	109.5956

	677.071
	20.41576
	677.494
	32.47645
	677.313
	78.74722
	677.313
	112.1724
	677.313
	190.5089
	677.313
	75.85506
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	21.13314
	741.233
	61.71618
	741.233
	158.1296
	741.233
	-4.73788
	741.233
	67.77865
	741.233
	27.03322

	741.596
	13.00218
	742.107
	33.90609
	741.957
	21.04102
	741.957
	60.8167
	741.957
	157.9172
	741.957
	-5.9787
	741.957
	67.10217
	741.957
	25.85791

	742.317
	12.96003
	742.829
	32.62427
	742.68
	21.25237
	742.68
	59.8911
	742.68
	158.9427
	742.68
	-7.24519
	742.68
	67.66421
	742.68
	24.98757

	743.038
	12.91259
	743.552
	33.25609
	743.402
	21.83598
	743.402
	59.37896
	743.402
	158.8607
	743.402
	-8.09773
	743.402
	67.11931
	743.402
	24.49099

	743.761
	12.86049
	744.274
	31.58845
	744.125
	21.6604
	744.125
	58.95403
	744.125
	157.5682
	744.125
	-8.86354
	744.125
	65.36335
	744.125
	23.23372

	744.482
	12.80433
	744.997
	32.29318
	744.848
	20.82877
	744.848
	58.36652
	744.848
	155.9022
	744.848
	-9.79193
	744.848
	63.23389
	744.848
	21.3204

	745.203
	12.74511
	745.719
	32.452
	745.571
	20.66227
	745.571
	57.60095
	745.571
	155.1311
	745.571
	-10.8984
	745.571
	61.9994
	745.571
	20.0722

	745.924
	12.68438
	746.441
	32.20091
	746.293
	19.66338
	746.293
	56.68659
	746.293
	152.8186
	746.293
	-12.1531
	746.293
	59.2241
	746.293
	17.99313

	746.646
	12.62281
	747.163
	31.47645
	747.015
	19.19532
	747.015
	54.78692
	747.015
	150.208
	747.015
	-14.3932
	747.015
	56.15063
	747.015
	16.44487

	747.367
	12.56059
	747.885
	31.21864
	747.737
	18.90945
	747.737
	54.56197
	747.737
	148.2429
	747.737
	-14.9586
	747.737
	53.72278
	747.737
	15.07881

	748.087
	12.49766
	748.607
	31.73927
	748.461
	19.02311
	748.461
	53.5327
	748.461
	145.3289
	748.461
	-16.3292
	748.461
	50.34463
	748.461
	14.10929

	748.808
	12.43465
	749.329
	29.83409
	749.183
	19.26989
	749.183
	52.52816
	749.183
	142.9834
	749.183
	-17.6741
	749.183
	47.53635
	749.183
	13.27587

	749.53
	12.37342
	750.051
	29.365
	749.905
	18.87276
	749.905
	51.83965
	749.905
	141.35
	749.905
	-18.703
	749.905
	45.44008
	749.905
	11.79854

	750.251
	12.31506
	750.773
	29.77273
	750.627
	18.25452
	750.627
	49.98885
	750.627
	139.2396
	750.627
	-20.8943
	750.627
	42.86689
	750.627
	10.10011

	750.971
	12.26042
	751.495
	29.08518
	751.35
	18.10526
	751.35
	49.63108
	751.35
	136.7276
	751.35
	-21.5929
	751.35
	39.89147
	751.35
	8.86917

	751.691
	12.20873
	752.217
	30.10209
	752.072
	17.20299
	752.072
	48.7156
	752.072
	135.3008
	752.072
	-22.8488
	752.072
	38.00186
	752.072
	6.88669

	752.412
	12.16061
	752.938
	29.30091
	752.793
	16.55315
	752.793
	47.39178
	752.793
	132.9817
	752.793
	-24.5125
	752.793
	35.22057
	752.793
	5.15816

	753.133
	12.11418
	753.66
	29.61073
	753.515
	16.58037
	753.515
	45.88792
	753.515
	130.4742
	753.515
	-26.3568
	753.515
	32.25027
	753.515
	4.10519

	753.853
	12.06972
	754.38
	29.53036
	754.236
	16.14337
	754.236
	44.76651
	754.236
	128.027
	754.236
	-27.8181
	754.236
	29.34084
	754.236
	2.58949

	754.574
	12.02807
	755.102
	30.13209
	754.959
	15.73251
	754.959
	43.52423
	754.959
	125.2032
	754.959
	-29.4013
	754.959
	26.05361
	754.959
	1.09694

	755.294
	11.99035
	755.823
	31.01345
	755.681
	15.40649
	755.681
	41.74428
	755.681
	121.7762
	755.681
	-31.5217
	755.681
	22.16379
	755.681
	-0.30927

	756.014
	11.95729
	756.544
	29.75427
	756.402
	14.21448
	756.402
	40.90245
	756.402
	119.4932
	756.402
	-32.7034
	756.402
	19.41856
	756.402
	-2.57998

	756.735
	11.92997
	757.265
	30.99291
	757.123
	13.00229
	757.123
	40.0273
	757.123
	117.9732
	757.123
	-33.9185
	757.123
	17.43643
	757.123
	-4.87086

	757.455
	11.90828
	757.987
	31.32445
	757.844
	12.60444
	757.844
	38.66917
	757.844
	113.841
	757.844
	-35.6166
	757.844
	12.84203
	757.844
	-6.34742

	758.174
	11.89237
	758.708
	32.93745
	758.567
	12.36884
	758.567
	38.88987
	758.567
	110.0035
	758.567
	-35.7367
	758.567
	8.54113
	758.567
	-7.66471

	758.894
	11.8835
	759.429
	34.38345
	759.288
	11.92066
	759.288
	37.48316
	759.288
	107.235
	759.288
	-37.4834
	759.288
	5.31038
	759.288
	-9.19158

	759.614
	11.88353
	760.15
	34.18691
	760.009
	9.87623
	760.009
	35.27841
	760.009
	103.5267
	760.009
	-40.0281
	760.009
	1.13997
	760.009
	-12.3147

	760.335
	11.8928
	760.87
	33.59509
	760.73
	9.0187
	760.73
	33.2776
	760.73
	100.5398
	760.73
	-42.3688
	760.73
	-2.30914
	760.73
	-14.2509

	761.054
	11.91204
	761.591
	31.92164
	761.45
	9.45185
	761.45
	31.68805
	761.45
	98.43993
	761.45
	-44.2978
	761.45
	-4.87052
	761.45
	-14.895

	761.774
	11.94406
	762.312
	31.70255
	762.171
	7.90688
	762.171
	29.71109
	762.171
	95.08811
	762.171
	-46.6147
	762.171
	-8.68452
	762.171
	-17.5187

	762.493
	11.99054
	763.033
	30.14264
	762.893
	6.41598
	762.893
	27.24911
	762.893
	92.36726
	762.893
	-49.4171
	762.893
	-11.8682
	762.893
	-20.0898

	763.212
	12.05158
	763.753
	29.76209
	763.614
	6.09536
	763.614
	25.93195
	763.614
	90.68964
	763.614
	-51.0742
	763.614
	-14.008
	763.614
	-21.4891

	763.931
	12.13002
	764.474
	30.43691
	764.334
	5.88073
	764.334
	23.70001
	764.334
	88.69074
	764.334
	-53.6456
	764.334
	-16.4684
	764.334
	-22.7809

	764.651
	12.22797
	765.193
	29.67055
	765.055
	5.4615
	765.055
	22.75085
	765.055
	85.86946
	765.055
	-54.9347
	765.055
	-19.7519
	765.055
	-24.2788

	765.371
	12.34665
	765.913
	27.20436
	765.775
	5.10843
	765.775
	22.17513
	765.775
	83.10652
	765.775
	-55.8499
	765.775
	-22.9763
	765.775
	-25.7091

	766.09
	12.48761
	766.634
	24.59955
	766.496
	3.27097
	766.496
	20.1863
	766.496
	80.44004
	766.496
	-58.1787
	766.496
	-26.105
	766.496
	-28.6253

	766.809
	12.6521
	767.354
	22.31364
	767.217
	2.73728
	767.217
	20.18911
	767.217
	76.75632
	767.217
	-58.5158
	767.217
	-30.2509
	767.217
	-30.2376

	767.528
	12.84126
	768.074
	21.66591
	767.938
	2.42399
	767.938
	19.29129
	767.938
	73.32193
	767.938
	-59.7535
	767.938
	-34.1475
	767.938
	-31.6296

	768.247
	13.05642
	768.794
	22.35191
	768.658
	2.23687
	768.658
	18.42572
	768.658
	70.99687
	768.658
	-60.9586
	768.658
	-36.934
	768.658
	-32.894

	768.965
	13.29716
	769.514
	22.30791
	769.378
	2.26821
	769.378
	17.02482
	769.378
	68.90743
	769.378
	-62.6989
	769.378
	-39.485
	769.378
	-33.9398

	769.684
	13.56296
	770.234
	21.17209
	770.098
	1.53526
	770.098
	15.34473
	770.098
	65.09587
	770.098
	-64.7185
	770.098
	-43.7581
	770.098
	-35.75

	770.404
	13.85152
	770.954
	22.07918
	770.818
	-0.2451
	770.818
	14.09827
	770.818
	59.95118
	770.818
	-66.3044
	770.818
	-49.3643
	770.818
	-38.6075

	771.122
	14.16169
	771.674
	20.40845
	771.537
	-0.47714
	771.537
	13.84651
	771.537
	56.84639
	771.537
	-66.8952
	771.537
	-52.93
	771.537
	-39.9153

	771.841
	14.49103
	772.392
	17.99491
	772.257
	-1.94902
	772.257
	12.60865
	772.257
	53.29106
	772.257
	-68.4725
	772.257
	-56.9469
	772.257
	-42.4644

	772.559
	14.83708
	773.112
	18.61591
	772.978
	-3.09232
	772.978
	10.84997
	772.978
	48.3777
	772.978
	-70.5711
	772.978
	-62.3224
	772.978
	-44.6864

	773.278
	15.1969
	773.832
	19.24073
	773.698
	-4.33121
	773.698
	9.56054
	773.698
	43.29944
	773.698
	-72.2
	773.698
	-67.8622
	773.698
	-47.0024

	773.996
	15.56862
	774.551
	19.54764
	774.418
	-5.05869
	774.418
	9.87612
	774.418
	39.60333
	774.418
	-72.2239
	774.418
	-72.0199
	774.418
	-48.8071

	774.714
	15.95028
	775.271
	20.99064
	775.137
	-5.48805
	775.137
	9.14147
	775.137
	37.80198
	775.137
	-73.2975
	775.137
	-74.2821
	775.137
	-50.3122

	775.432
	16.34025
	775.99
	21.26155
	775.857
	-5.93334
	775.857
	8.68971
	775.857
	36.00847
	775.857
	-74.0887
	775.857
	-76.5371
	775.857
	-51.8347

	776.15
	16.7359
	776.71
	20.12318
	776.576
	-5.24324
	776.576
	8.04541
	776.576
	32.90683
	776.576
	-75.072
	776.576
	-80.0997
	776.576
	-52.2203

	776.869
	17.13417
	777.427
	19.57082
	777.295
	-4.66369
	777.295
	7.24105
	777.295
	29.03567
	777.295
	-76.2154
	777.295
	-84.4317
	777.295
	-52.7164

	777.587
	17.53328
	778.147
	19.025
	778.014
	-4.56313
	778.014
	6.64226
	778.014
	26.38133
	778.014
	-77.1532
	778.014
	-87.547
	778.014
	-53.6916

	778.305
	17.93207
	778.866
	18.792
	778.734
	-4.63498
	778.734
	5.31973
	778.734
	23.51724
	778.734
	-78.8151
	778.734
	-90.8726
	778.734
	-54.8406

	779.023
	18.32854
	779.585
	18.88564
	779.454
	-4.81974
	779.454
	4.43825
	779.454
	19.08487
	779.454
	-80.0361
	779.454
	-95.7665
	779.454
	-56.1026

	779.741
	18.72037
	780.304
	19.79255
	780.173
	-5.33205
	780.173
	3.08167
	780.173
	15.23318
	780.173
	-81.7317
	780.173
	-100.079
	780.173
	-57.6906

	780.458
	19.10732
	781.023
	19.242
	780.892
	-5.24669
	780.892
	2.39499
	780.892
	12.84992
	780.892
	-82.7573
	780.892
	-102.923
	780.892
	-58.681

	781.176
	19.48921
	781.74
	20.58782
	781.611
	-4.73757
	781.611
	2.14824
	781.611
	11.16554
	781.611
	-83.3431
	781.611
	-105.069
	781.611
	-59.2475

	781.893
	19.86446
	782.459
	19.98855
	782.33
	-3.72391
	782.33
	1.74904
	782.33
	8.62351
	782.33
	-84.0813
	782.33
	-108.071
	782.33
	-59.3096

	782.611
	20.08968
	783.178
	17.52245
	783.049
	-1.54553
	783.049
	1.71694
	783.049
	5.51707
	783.049
	-84.4524
	783.049
	-111.639
	783.049
	-58.2069

	783.328
	20.31137
	783.897
	18.04527
	783.767
	-1.15763
	783.767
	1.27977
	783.767
	3.79725
	783.767
	-85.228
	783.767
	-113.819
	783.767
	-58.8932

	784.045
	20.5296
	784.615
	18.14218
	784.486
	-1.35507
	784.486
	1.06594
	784.486
	2.31773
	784.486
	-85.7809
	784.486
	-115.759
	784.486
	-60.1664

	784.763
	20.7442
	785.334
	19.24727
	785.204
	-2.02672
	785.204
	1.18664
	785.204
	2.21658
	785.204
	-85.9987
	785.204
	-116.321
	785.204
	-61.9122

	785.48
	20.95533
	786.051
	20.40727
	785.923
	-1.24351
	785.923
	0.62967
	785.923
	0
	785.923
	-86.8946
	785.923
	-118.998
	785.923
	-62.2047

	786.197
	21.16335
	786.769
	20.53845
	786.641
	0
	786.641
	0
	786.641
	-1.49147
	786.641
	-87.8628
	786.641
	-120.238
	786.641
	-62.0354

	786.914
	21.36834
	787.488
	20.32045
	787.36
	0.16626
	787.36
	-1.14382
	787.36
	-3.36001
	787.36
	-88.5251
	787.36
	-121.854
	787.36
	-61.2863

	787.631
	21.57044
	788.206
	20.11145
	788.078
	-0.80469
	788.078
	-3.12651
	788.078
	-6.16472
	788.078
	-90.0268
	788.078
	-124.407
	788.078
	-61.6752

	788.348
	21.76975
	788.924
	19.252
	788.796
	-1.56777
	788.796
	-4.24635
	788.796
	-7.26531
	788.796
	-90.6658
	788.796
	-125.256
	788.796
	-61.8562

	789.066
	21.96643
	789.641
	16.88718
	789.514
	-2.50768
	789.514
	-5.25551
	789.514
	-7.80609
	789.514
	-91.194
	789.514
	-125.545
	789.514
	-62.214

	789.783
	22.16033
	790.359
	16.34391
	790.232
	-4.07366
	790.232
	-6.3754
	790.232
	-9.79814
	790.232
	-91.833
	790.232
	-127.286
	790.232
	-63.198

	790.499
	22.35137
	791.077
	16.77745
	790.95
	-4.31509
	790.95
	-6.12264
	790.95
	-10.5908
	790.95
	-91.0993
	790.95
	-127.827
	790.95
	-62.8573

	791.216
	22.53991
	791.795
	16.59
	791.668
	-5.12336
	791.668
	-5.22114
	791.668
	-13.2181
	791.668
	-89.7169
	791.668
	-130.202
	791.668
	-63.0835

	791.932
	22.72599
	792.511
	16.66282
	792.386
	-5.00042
	792.386
	-4.88129
	792.386
	-13.4534
	792.386
	-88.8961
	792.386
	-130.186
	792.386
	-62.3785

	792.649
	22.90964
	793.229
	14.40373
	793.105
	-3.97728
	793.105
	-4.89457
	793.105
	-14.5472
	793.105
	-88.4278
	793.105
	-131.028
	793.105
	-60.7725

	793.365
	23.0911
	793.947
	14.53009
	793.823
	-2.95507
	793.823
	-5.12868
	793.823
	-14.8772
	793.823
	-88.181
	793.823
	-131.106
	793.823
	-59.1683

	794.082
	23.27052
	794.664
	13.28645
	794.541
	-3.20872
	794.541
	-4.79817
	794.541
	-14.3822
	794.541
	-87.3695
	794.541
	-130.359
	794.541
	-58.8398

	794.798
	23.44826
	795.382
	13.41182
	795.258
	-2.72879
	795.258
	-5.49476
	795.258
	-14.6116
	795.258
	-87.5859
	795.258
	-130.337
	795.258
	-57.7787

	795.514
	23.62415
	796.098
	14.078
	795.976
	-2.45906
	795.976
	-4.6647
	795.976
	-14.5379
	795.976
	-86.2749
	795.976
	-130.012
	795.976
	-56.9269

	796.23
	23.79847
	796.816
	14.21682
	796.693
	-1.04987
	796.693
	-3.48252
	796.693
	-14.7313
	796.693
	-84.6125
	796.693
	-129.954
	796.693
	-54.9364

	796.469
	23.97133
	797.533
	15.339
	797.411
	-0.76381
	797.411
	-2.58012
	797.411
	-14.3149
	797.411
	-83.2291
	797.411
	-129.286
	797.411
	-54.0683

	797.187
	24.14312
	798.25
	14.84973
	798.128
	0.0731
	798.128
	-1.65887
	798.128
	-15.2182
	798.128
	-81.8276
	798.128
	-129.938
	798.128
	-52.6502

	797.905
	24.31388
	798.966
	14.757
	798.845
	1.21944
	798.845
	0.12346
	798.845
	-15.2932
	798.845
	-79.565
	798.845
	-129.761
	798.845
	-50.9226

	798.623
	24.48374
	799.683
	13.20055
	799.562
	2.05444
	799.562
	1.73607
	799.562
	-15.0952
	799.562
	-77.4722
	799.562
	-129.312
	799.562
	-49.5063

	799.341
	24.65285
	800.4
	11.51673
	800.279
	2.84378
	800.279
	2.707
	800.279
	-14.3776
	800.279
	-76.021
	800.279
	-128.343
	800.279
	-48.1357

	800.058
	24.82141
	801.117
	13.83191
	800.997
	2.75508
	800.997
	4.01244
	800.997
	-14.1015
	800.997
	-74.2346
	800.997
	-127.815
	800.997
	-47.6424

	800.777
	24.9895
	801.833
	14.43727
	801.714
	4.13505
	801.714
	5.70983
	801.714
	-14.0216
	801.714
	-72.057
	801.714
	-127.484
	801.714
	-45.6811
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	862.936
	29.06101
	863.898
	11.46164
	863.808
	94.55326
	863.808
	85.23398
	863.808
	124.6523
	863.808
	49.05816
	863.808
	32.95705
	863.808
	95.0748

	863.648
	29.00657
	864.608
	10.59873
	864.519
	92.16025
	864.519
	82.11542
	864.519
	121.0444
	864.519
	46.41584
	864.519
	29.59839
	864.519
	93.25817

	864.359
	28.95367
	865.319
	9.92255
	865.229
	89.40454
	865.229
	78.25918
	865.229
	116.1721
	865.229
	43.03516
	865.229
	24.97497
	865.229
	91.07804

	865.069
	28.90212
	866.028
	9.59509
	865.94
	86.57549
	865.94
	75.63074
	865.94
	110.5578
	865.94
	40.88296
	865.94
	19.60989
	865.94
	88.82538

	865.78
	28.85211
	866.738
	8.82091
	866.65
	83.60768
	866.65
	73.12921
	866.65
	106.5464
	866.65
	38.85698
	866.65
	15.84746
	866.65
	86.43315

	866.491
	28.80357
	867.448
	8.84691
	867.36
	80.9546
	867.36
	70.26519
	867.36
	102.62
	867.36
	36.46853
	867.36
	12.16988
	867.36
	84.35564

	867.203
	28.75657
	868.157
	10.45455
	868.07
	79.07548
	868.07
	67.26307
	868.07
	96.66196
	868.07
	33.94197
	868.07
	6.46078
	868.07
	83.0521

	867.914
	28.71076
	868.868
	10.05364
	868.781
	75.75145
	868.781
	63.06346
	868.781
	90.77136
	868.781
	30.2186
	868.781
	0.81943
	868.781
	80.30445

	868.624
	28.66577
	869.577
	9.33173
	869.49
	72.07377
	869.49
	60.52983
	869.49
	85.83623
	869.49
	28.15986
	869.49
	-3.86716
	869.49
	77.20154

	869.335
	28.62139
	870.286
	8.02727
	870.201
	68.76431
	870.201
	57.74081
	870.201
	81.61681
	870.201
	25.84707
	870.201
	-7.83733
	870.201
	74.46846

	870.045
	28.5778
	870.997
	6.27873
	870.91
	65.75569
	870.91
	55.92593
	870.91
	76.96839
	870.91
	24.50708
	870.91
	-12.2372
	870.91
	72.0346

	870.756
	28.53517
	871.706
	5.77418
	871.62
	61.38316
	871.62
	53.23422
	871.62
	72.073
	871.62
	22.29094
	871.62
	-16.8837
	871.62
	68.23765

	871.466
	28.49339
	872.416
	5.91664
	872.33
	58.14105
	872.33
	50.61869
	872.33
	67.67115
	872.33
	20.15097
	872.33
	-21.0367
	872.33
	65.57112

	872.176
	28.45241
	873.125
	5.52227
	873.039
	55.36723
	873.039
	44.9008
	873.039
	62.10435
	873.039
	14.90797
	873.039
	-26.3549
	873.039
	63.37206

	872.888
	28.41188
	873.833
	3.97373
	873.749
	51.5536
	873.749
	41.58562
	873.749
	59.42769
	873.749
	12.06835
	873.749
	-28.7827
	873.749
	60.13401

	873.598
	28.37166
	874.543
	3.92918
	874.459
	48.03686
	874.459
	38.79056
	874.459
	54.07226
	874.459
	9.74886
	874.459
	-33.8892
	874.459
	57.19285

	874.308
	28.33156
	875.252
	4.98018
	875.168
	46.02077
	875.168
	36.40587
	875.168
	50.38993
	875.168
	7.83907
	875.168
	-37.323
	875.168
	55.75152

	875.018
	28.29153
	875.96
	5.27882
	875.878
	43.03625
	875.878
	33.96944
	875.878
	46.42882
	875.878
	5.8782
	875.878
	-41.0352
	875.878
	53.34257

	875.728
	28.25108
	876.67
	5.40709
	876.587
	39.80295
	876.587
	31.0318
	876.587
	41.80742
	876.587
	3.41545
	876.587
	-45.4081
	876.587
	50.68404

	876.438
	28.21033
	877.379
	5.97864
	877.296
	37.2191
	877.296
	28.90091
	877.296
	38.76641
	877.296
	1.75946
	877.296
	-48.2006
	877.296
	48.67495

	877.148
	28.16882
	878.088
	7.26645
	878.005
	35.20543
	878.005
	28.11778
	878.005
	35.55403
	878.005
	1.45122
	878.005
	-51.1644
	878.005
	47.23605

	877.857
	28.12632
	878.797
	7.425
	878.714
	30.82568
	878.714
	24.23606
	878.714
	32.96724
	878.714
	-1.95561
	878.714
	-53.5026
	878.714
	43.43106

	878.567
	28.08281
	879.505
	8.18955
	879.423
	28.6695
	879.423
	22.23291
	879.423
	29.37011
	879.423
	-3.48387
	879.423
	-56.8512
	879.423
	41.84965

	879.278
	28.03812
	880.214
	6.92682
	880.133
	26.03093
	880.133
	21.0017
	880.133
	28.73553
	880.133
	-4.23951
	880.133
	-57.2369
	880.133
	39.78665

	879.987
	27.99205
	880.922
	5.71164
	880.841
	24.04968
	880.841
	18.61975
	880.841
	25.21103
	880.841
	-6.14724
	880.841
	-60.5132
	880.841
	38.37936

	880.697
	27.94427
	881.63
	6.79227
	881.55
	21.76843
	881.55
	16.89919
	881.55
	23.08679
	881.55
	-7.3929
	881.55
	-62.3889
	881.55
	36.67287

	881.406
	27.89462
	882.34
	5.85291
	882.258
	19.09016
	882.258
	15.27618
	882.258
	21.01196
	882.258
	-8.54169
	882.258
	-64.2156
	882.258
	34.56856

	882.115
	27.84292
	883.047
	5.11109
	882.967
	16.98267
	882.967
	12.59683
	882.967
	19.7815
	882.967
	-10.7462
	882.967
	-65.1975
	882.967
	33.03583

	882.825
	27.78895
	883.755
	3.76427
	883.677
	15.79049
	883.677
	11.27702
	883.677
	17.73487
	883.677
	-11.5904
	883.677
	-66.9952
	883.677
	32.41923

	883.534
	27.73282
	884.464
	3.21164
	884.384
	14.4821
	884.384
	10.17411
	884.384
	13.93394
	884.384
	-12.2198
	884.384
	-70.5483
	884.384
	31.68398

	884.243
	27.6746
	885.172
	3.24945
	885.093
	12.18351
	885.093
	8.3587
	885.093
	10.69393
	885.093
	-13.5603
	885.093
	-73.5398
	885.093
	29.96016

	884.952
	27.61404
	885.88
	2.99291
	885.801
	10.87848
	885.801
	6.7412
	885.801
	8.54465
	885.801
	-14.7035
	885.801
	-75.4409
	885.801
	29.22908

	885.661
	27.5512
	886.589
	2.598
	886.51
	9.06818
	886.51
	7.13815
	886.51
	7.51212
	886.51
	-13.8317
	886.51
	-76.2248
	886.51
	27.99354

	886.37
	27.4858
	887.296
	1.66091
	887.217
	7.33186
	887.217
	5.90626
	887.217
	7.20424
	887.217
	-14.59
	887.217
	-76.2849
	887.217
	26.83037

	887.079
	27.41753
	888.003
	1.51309
	887.926
	6.35789
	887.926
	5.38655
	887.926
	6.26233
	887.926
	-14.6349
	887.926
	-76.9783
	887.926
	26.43116

	887.787
	27.34626
	888.711
	2.16709
	888.635
	6.17922
	888.635
	4.87686
	888.635
	3.7481
	888.635
	-14.6697
	888.635
	-79.2439
	888.635
	26.82726

	888.496
	27.27208
	889.419
	1.78336
	889.342
	4.31518
	889.342
	3.21716
	889.342
	2.55092
	889.342
	-15.8558
	889.342
	-80.1933
	889.342
	25.53636

	889.205
	27.19488
	890.126
	3.366
	890.05
	2.18527
	890.05
	2.11601
	890.05
	2.83932
	890.05
	-16.4827
	890.05
	-79.6567
	890.05
	23.98041

	889.915
	27.11498
	890.834
	2.83918
	890.758
	2.37635
	890.758
	0.90133
	890.758
	1.18869
	890.758
	-17.2232
	890.758
	-81.0591
	890.758
	24.74544

	890.623
	27.03266
	891.542
	3.08418
	891.466
	1.7624
	891.466
	0.68471
	891.466
	0.63244
	891.466
	-16.9656
	891.466
	-81.3672
	891.466
	24.70545

	891.332
	26.94845
	892.249
	3.88718
	892.173
	1.05378
	892.173
	0.81502
	892.173
	-1.01818
	892.173
	-16.3617
	892.173
	-82.77
	892.173
	24.56997

	892.04
	26.86254
	892.956
	4.17127
	892.881
	-1.0559
	892.881
	-1.08215
	892.881
	0.64529
	892.881
	-17.7847
	892.881
	-80.8583
	892.881
	23.32476

	892.748
	26.77548
	893.664
	3.44655
	893.588
	-1.69472
	893.588
	-0.0318
	893.588
	0.06224
	893.588
	-16.2608
	893.588
	-81.1935
	893.588
	23.9486

	893.457
	26.68757
	894.371
	4.191
	894.296
	-2.27705
	894.296
	-0.93024
	894.296
	-1.07466
	894.296
	-15.6855
	894.296
	-81.1432
	894.296
	24.63072

	894.165
	26.59867
	895.078
	4.884
	895.003
	-3.1205
	895.003
	-2.17063
	895.003
	-2.43149
	895.003
	-14.9961
	895.003
	-80.884
	895.003
	25.04993

	894.873
	26.50923
	895.784
	5.55827
	895.711
	-4.46823
	895.711
	-3.87902
	895.711
	-4.00111
	895.711
	-14.7719
	895.711
	-80.8353
	895.711
	24.96665

	895.581
	26.41954
	896.492
	4.72145
	896.419
	-5.26612
	896.419
	-5.01821
	896.419
	-5.44112
	896.419
	-13.9786
	896.419
	-80.6571
	896.419
	25.43321

	896.289
	26.33002
	897.199
	4.46818
	897.125
	-6.41214
	897.125
	-6.74152
	897.125
	-6.81139
	897.125
	-13.7748
	897.125
	-80.4136
	897.125
	25.54806

	896.997
	26.24082
	897.905
	2.64918
	897.833
	-6.73677
	897.833
	-7.40929
	897.833
	-6.66967
	897.833
	-12.5101
	897.833
	-78.6536
	897.833
	26.48788

	897.704
	26.15217
	898.612
	2.81509
	898.54
	-7.19565
	898.54
	-8.33235
	898.54
	-7.30523
	898.54
	-11.5033
	898.54
	-77.6732
	898.54
	27.29167

	898.412
	26.06436
	899.319
	3.15709
	899.247
	-8.00114
	899.247
	-9.10581
	899.247
	-8.38507
	899.247
	-10.347
	899.247
	-77.137
	899.247
	27.74883

	899.12
	25.9776
	900.025
	2.66927
	899.954
	-8.76147
	899.954
	-10.274
	899.954
	-7.9462
	899.954
	-9.58534
	899.954
	-75.0821
	899.954
	28.25116

	899.828
	25.89217
	900.732
	1.03227
	900.661
	-8.79861
	900.661
	-10.9386
	900.661
	-7.18691
	900.661
	-8.32016
	900.661
	-72.7069
	900.661
	29.47669

	900.535
	25.80833
	901.438
	1.60282
	901.367
	-9.31682
	901.367
	-10.9326
	901.367
	-6.53008
	901.367
	-6.38709
	901.367
	-70.4363
	901.367
	30.21936

	901.243
	25.72593
	902.145
	3.139
	902.075
	-8.71228
	902.075
	-10.7969
	902.075
	-4.64758
	902.075
	-4.3189
	902.075
	-66.9355
	902.075
	32.08834

	901.95
	25.64496
	902.851
	4.15764
	902.781
	-8.34432
	902.781
	-10.9527
	902.781
	-4.21013
	902.781
	-2.5476
	902.781
	-64.8844
	902.781
	33.71718

	902.657
	25.56579
	903.557
	4.79282
	903.488
	-8.23534
	903.488
	-11.1676
	903.488
	-2.73371
	903.488
	-0.83276
	903.488
	-61.7919
	903.488
	35.08882

	903.365
	25.48872
	904.263
	4.957
	904.194
	-8.3294
	904.194
	-11.1838
	904.194
	-1.17451
	904.194
	1.07819
	904.194
	-58.619
	904.194
	36.25564

	904.072
	25.41417
	904.97
	5.59918
	904.901
	-8.27338
	904.901
	-9.70745
	904.901
	0.06138
	904.901
	4.48429
	904.901
	-55.7671
	904.901
	37.57432

	904.779
	25.34226
	905.676
	7.25455
	905.607
	-8.14575
	905.607
	-9.80377
	905.607
	2.32633
	905.607
	6.31503
	905.607
	-51.8885
	905.607
	38.96282

	905.486
	25.27311
	906.381
	7.49309
	906.314
	-7.53688
	906.314
	-10.8263
	906.314
	4.91346
	906.314
	7.2223
	906.314
	-47.6853
	906.314
	40.83436

	906.193
	25.20675
	907.087
	7.52373
	907.019
	-7.29262
	907.019
	-10.9471
	907.019
	6.9372
	907.019
	9.02586
	907.019
	-44.0502
	907.019
	42.33771

	906.9
	25.14365
	907.792
	8.37945
	907.725
	-6.63927
	907.725
	-11.2204
	907.725
	8.42871
	907.725
	10.67961
	907.725
	-40.9449
	907.725
	44.25193

	907.606
	25.08381
	908.499
	9.23082
	908.432
	-6.67861
	908.432
	-11.3421
	908.432
	10.22628
	908.432
	12.48771
	908.432
	-37.5314
	908.432
	45.47525

	908.312
	25.02726
	909.205
	8.42982
	909.137
	-6.26727
	909.137
	-8.4707
	909.137
	11.87766
	909.137
	17.28345
	909.137
	-34.2686
	909.137
	47.14569

	909.019
	24.97444
	909.91
	6.10373
	909.844
	-5.18802
	909.844
	-8.91059
	909.844
	12.23642
	909.844
	18.77335
	909.844
	-32.2938
	909.844
	49.48761

	909.726
	24.9254
	910.615
	5.102
	910.549
	-3.58632
	910.549
	-8.59035
	910.549
	14.06444
	910.549
	21.01794
	910.549
	-28.8544
	910.549
	52.34839

	910.432
	24.88013
	911.32
	5.12491
	911.255
	-3.45907
	911.255
	-8.39516
	911.255
	14.89615
	911.255
	23.14019
	911.255
	-26.4089
	911.255
	53.73652

	911.139
	24.83865
	912.027
	6.087
	911.961
	-4.18152
	911.961
	-7.73053
	911.961
	15.6931
	911.961
	25.73188
	911.961
	-23.9983
	911.961
	54.27495

	911.846
	24.80107
	912.732
	6.53273
	912.667
	-4.34156
	912.667
	-7.03336
	912.667
	18.14557
	912.667
	28.35612
	912.667
	-19.9321
	912.667
	55.37578

	912.552
	24.76716
	913.437
	5.96864
	913.372
	-3.36265
	913.372
	-7.23343
	913.372
	19.03378
	913.372
	30.08039
	913.372
	-17.4325
	913.372
	57.61378

	913.258
	24.73699
	914.142
	6.78873
	914.078
	-2.67307
	914.078
	-8.90209
	914.078
	19.6859
	914.078
	30.3388
	914.078
	-15.1666
	914.078
	59.56424

	913.965
	24.71033
	914.847
	6.20836
	914.783
	-1.62805
	914.783
	-7.77133
	914.783
	19.96374
	914.783
	33.3939
	914.783
	-13.2774
	914.783
	61.86834

	914.671
	24.6871
	915.551
	5.13464
	915.488
	-1.30472
	915.488
	-6.90939
	915.488
	21.58794
	915.488
	36.18018
	915.488
	-10.0417
	915.488
	63.45077

	915.377
	24.66723
	916.257
	5.38127
	916.194
	1.07168
	916.194
	-6.41582
	916.194
	21.00611
	916.194
	38.60082
	916.194
	-9.00985
	916.194
	67.08804

	916.083
	24.65059
	916.962
	5.81682
	916.899
	1.76599
	916.899
	-5.68228
	916.899
	21.92593
	916.899
	41.25869
	916.899
	-6.4786
	916.899
	69.04145

	916.789
	24.63701
	917.667
	7.41773
	917.604
	1.73317
	917.604
	-5.00402
	917.604
	22.31703
	917.604
	43.86129
	917.604
	-4.47606
	917.604
	70.26771

	917.495
	24.62637
	918.371
	7.188
	918.309
	3.84009
	918.309
	-4.65326
	918.309
	24.0897
	918.309
	46.13639
	918.309
	-1.09197
	918.309
	73.63373

	918.199
	24.61896
	919.076
	6.467
	919.013
	4.99494
	919.013
	-2.51972
	919.013
	23.98126
	919.013
	50.19154
	919.013
	0.40874
	919.013
	76.04587

	918.905
	24.61488
	919.78
	6.15918
	919.719
	4.96789
	919.719
	-1.62937
	919.719
	24.80719
	919.719
	53.00896
	919.719
	2.84838
	919.719
	77.2797

	919.611
	24.61419
	920.486
	4.34782
	920.424
	5.51532
	920.424
	-0.2332
	920.424
	26.66304
	920.424
	56.32946
	920.424
	6.31565
	920.424
	79.08623

	920.317
	24.61691
	921.19
	3.52055
	921.129
	7.46634
	921.129
	1.27184
	921.129
	28.75766
	921.129
	59.75884
	921.129
	10.0217
	921.129
	82.29633

	921.022
	24.62304
	921.894
	1.73
	921.833
	9.1081
	921.833
	3.20269
	921.833
	29.75652
	921.833
	63.6113
	921.833
	12.6297
	921.833
	85.1954

	921.728
	24.63227
	922.598
	1.77427
	922.537
	10.30388
	922.537
	2.47696
	922.537
	30.59658
	922.537
	64.80718
	922.537
	15.07891
	922.537
	87.64848

	922.433
	24.64464
	923.302
	2.537
	923.243
	12.15283
	923.243
	2.98016
	923.243
	31.22642
	923.243
	67.23745
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	1041.31
	25.54451
	1041.99
	-17.5896
	1041.99
	0.20785
	1041.99
	0.22356
	1041.99
	18.4958
	1041.99
	59.84805
	1041.99
	-30.5493
	1041.99
	20.31166

	1042
	25.51698
	1042.68
	-18.5108
	1042.68
	-0.92474
	1042.68
	-0.45282
	1042.68
	15.75038
	1042.68
	57.98139
	1042.68
	-34.5303
	1042.68
	17.88166

	1042.7
	25.49028
	1043.37
	-20.8179
	1043.37
	-2.43961
	1043.37
	-1.08395
	1043.37
	11.95455
	1043.37
	56.15996
	1043.37
	-39.5618
	1043.37
	15.06937

	1043.39
	25.46444
	1044.06
	-21.2354
	1044.07
	-4.10022
	1044.07
	-1.76875
	1044.07
	10.47115
	1044.07
	54.26762
	1044.07
	-42.2987
	1044.07
	12.09254

	1044.08
	25.43933
	1044.76
	-18.3834
	1044.76
	-7.03074
	1044.76
	-2.00222
	1044.76
	8.80473
	1044.76
	52.84386
	1044.76
	-45.2008
	1044.76
	7.8646

	1044.77
	25.41486
	1045.45
	-16.3016
	1045.45
	-8.08886
	1045.45
	-3.71996
	1045.45
	5.54874
	1045.45
	49.93584
	1045.45
	-49.6924
	1045.45
	5.50906

	1045.47
	25.39116
	1046.14
	-16.0126
	1046.14
	-7.95983
	1046.14
	-5.90644
	1046.14
	3.55038
	1046.14
	46.55906
	1046.14
	-52.9264
	1046.14
	4.34068

	1046.16
	25.36782
	1046.83
	-16.2869
	1046.84
	-9.32931
	1046.84
	-6.90789
	1046.84
	1.74309
	1046.84
	44.35007
	1046.84
	-55.9872
	1046.84
	1.65498

	1046.85
	25.34489
	1047.52
	-17.6508
	1047.53
	-11.3727
	1047.53
	-6.99516
	1047.53
	0.49966
	1047.53
	43.07251
	1047.53
	-58.4662
	1047.53
	-1.68584

	1047.55
	25.32227
	1048.22
	-17.8033
	1048.22
	-11.1047
	1048.22
	-7.67639
	1048.22
	-1.04339
	1048.22
	41.20099
	1048.22
	-61.2449
	1048.22
	-2.71523

	1048.24
	25.29972
	1048.91
	-17.1736
	1048.91
	-11.0061
	1048.91
	-8.65149
	1048.91
	-1.98467
	1048.91
	39.0356
	1048.91
	-63.4218
	1048.91
	-3.91406

	1048.93
	25.27751
	1049.6
	-16.2646
	1049.6
	-10.4293
	1049.6
	-8.86005
	1049.6
	-2.33515
	1049.6
	37.63675
	1049.6
	-65.0079
	1049.6
	-4.63467

	1049.62
	25.25591
	1050.29
	-15.8966
	1050.3
	-11.0589
	1050.3
	-9.82866
	1050.3
	-2.41637
	1050.3
	35.4606
	1050.3
	-66.3427
	1050.3
	-6.58052

	1050.32
	25.23482
	1050.98
	-14.5071
	1050.99
	-12.5233
	1050.99
	-11.8792
	1050.99
	-2.66862
	1050.99
	32.2198
	1050.99
	-67.8305
	1050.99
	-9.34228

	1051.01
	25.21417
	1051.67
	-15.8647
	1051.68
	-13.1012
	1051.68
	-12.4912
	1051.68
	-2.22557
	1051.68
	30.4175
	1051.68
	-68.6231
	1051.68
	-11.2176

	1051.7
	25.19396
	1052.36
	-18.392
	1052.37
	-12.9518
	1052.37
	-12.0117
	1052.37
	-3.32959
	1052.37
	29.70672
	1052.37
	-70.9627
	1052.37
	-12.3656

	1052.39
	25.1744
	1053.05
	-20.0238
	1053.06
	-12.3839
	1053.06
	-11.7527
	1053.06
	-2.65732
	1053.06
	28.77541
	1053.06
	-71.5261
	1053.06
	-13.0952

	1053.08
	25.15535
	1053.75
	-20.78
	1053.75
	-13.2811
	1053.75
	-11.6502
	1053.75
	-2.82449
	1053.75
	27.68758
	1053.75
	-72.9289
	1053.75
	-15.2898

	1053.78
	25.13698
	1054.44
	-21.3914
	1054.44
	-12.5195
	1054.44
	-10.7312
	1054.44
	-3.1954
	1054.44
	27.41631
	1054.44
	-74.5354
	1054.44
	-15.8255

	1054.47
	25.11906
	1055.13
	-22.0737
	1055.14
	-11.3543
	1055.14
	-11.5243
	1055.14
	-3.60369
	1055.14
	25.41568
	1055.14
	-76.1972
	1055.14
	-15.9766

	1055.16
	25.10162
	1055.82
	-22.6011
	1055.83
	-10.2603
	1055.83
	-10.9481
	1055.83
	-2.07321
	1055.83
	24.8016
	1055.83
	-75.9024
	1055.83
	-16.18

	1055.85
	25.08473
	1056.51
	-21.5246
	1056.52
	-9.86483
	1056.52
	-9.86684
	1056.52
	-1.32471
	1056.52
	24.69255
	1056.52
	-76.3895
	1056.52
	-17.082

	1056.54
	25.06857
	1057.2
	-22.7193
	1057.21
	-9.86923
	1057.21
	-9.18945
	1057.21
	-2.12345
	1057.21
	24.17966
	1057.21
	-78.4239
	1057.21
	-18.3838

	1057.24
	25.05297
	1057.89
	-21.9076
	1057.9
	-9.28836
	1057.9
	-8.37689
	1057.9
	-1.75355
	1057.9
	23.80192
	1057.9
	-79.2896
	1057.9
	-19.1004

	1057.93
	25.03789
	1058.58
	-21.7042
	1058.59
	-8.61889
	1058.59
	-7.16918
	1058.59
	-1.81345
	1058.59
	23.81935
	1058.59
	-80.5851
	1058.59
	-19.7283

	1058.62
	25.02317
	1059.27
	-19.704
	1059.28
	-7.95975
	1059.28
	-6.63876
	1059.28
	-1.81238
	1059.28
	23.15947
	1059.28
	-81.8197
	1059.28
	-20.3666

	1059.31
	25.00852
	1059.96
	-19.9538
	1059.97
	-7.51888
	1059.97
	-6.36907
	1059.97
	-1.24483
	1059.97
	22.23887
	1059.97
	-82.4877
	1059.97
	-21.2231

	1060
	24.99409
	1060.65
	-20.0141
	1060.66
	-8.30744
	1060.66
	-6.48696
	1060.66
	-1.75277
	1060.66
	20.93069
	1060.66
	-84.2313
	1060.66
	-23.3091

	1060.69
	24.97998
	1061.34
	-19.7873
	1061.35
	-9.35563
	1061.35
	-6.58891
	1061.35
	0.00988
	1061.35
	19.63846
	1061.35
	-83.7043
	1061.35
	-25.6547

	1061.39
	24.96595
	1062.03
	-18.5881
	1062.04
	-9.32573
	1062.04
	-7.67973
	1062.04
	0.77484
	1062.04
	17.35735
	1062.04
	-84.1749
	1062.04
	-26.9222

	1062.08
	24.95198
	1062.72
	-17.8958
	1062.74
	-9.68085
	1062.74
	-8.39713
	1062.74
	0.64082
	1062.74
	15.4324
	1062.74
	-85.5625
	1062.74
	-28.5936

	1062.77
	24.93811
	1063.41
	-18.0316
	1063.42
	-10.6722
	1063.42
	-8.1831
	1063.42
	-0.10275
	1063.42
	14.4734
	1063.42
	-87.5238
	1063.42
	-30.8636

	1063.46
	24.92406
	1064.1
	-18.8776
	1064.12
	-10.3774
	1064.12
	-7.20175
	1064.12
	0.4593
	1064.12
	14.2472
	1064.12
	-88.2152
	1064.12
	-31.8849

	1064.15
	24.90966
	1064.79
	-18.1114
	1064.81
	-10.6225
	1064.81
	-6.84711
	1064.81
	1.24772
	1064.81
	13.41155
	1064.81
	-88.6624
	1064.81
	-33.4275

	1064.84
	24.89502
	1065.48
	-17.5224
	1065.5
	-9.97567
	1065.5
	-5.40085
	1065.5
	0.66909
	1065.5
	13.66752
	1065.5
	-90.4767
	1065.5
	-34.078

	1065.53
	24.88027
	1066.17
	-17.6943
	1066.19
	-9.27689
	1066.19
	-6.37667
	1066.19
	0.61868
	1066.19
	11.50141
	1066.19
	-91.7627
	1066.19
	-34.6767

	1066.22
	24.86544
	1066.86
	-19.1714
	1066.88
	-7.83579
	1066.88
	-4.41243
	1066.88
	0.28338
	1066.88
	12.27536
	1066.88
	-93.3336
	1066.88
	-34.533

	1066.91
	24.85039
	1067.55
	-20.2257
	1067.57
	-5.88284
	1067.57
	-3.49399
	1067.57
	-0.54353
	1067.57
	12.00351
	1067.57
	-95.3962
	1067.57
	-33.8775

	1067.6
	24.83541
	1068.24
	-21.3046
	1068.26
	-5.8608
	1068.26
	-3.18757
	1068.26
	-0.19204
	1068.26
	11.11964
	1068.26
	-96.2803
	1068.26
	-35.1528

	1068.29
	24.82068
	1068.93
	-22.1975
	1068.95
	-5.14448
	1068.95
	-1.26421
	1068.95
	-0.51491
	1068.95
	11.85271
	1068.95
	-96.7793
	1068.95
	-35.7339

	1068.98
	24.80606
	1069.62
	-23.3337
	1069.64
	-4.6423
	1069.64
	0.45973
	1069.64
	-2.35651
	1069.64
	12.78681
	1069.64
	-98.4235
	1069.64
	-36.5292

	1069.68
	24.79127
	1070.31
	-23.9289
	1070.33
	-3.30466
	1070.33
	0.61735
	1070.33
	-3.16281
	1070.33
	12.74314
	1070.33
	-99.0323
	1070.33
	-36.4889

	1070.37
	24.77582
	1071
	-25.2123
	1071.02
	-2.97278
	1071.02
	2.48191
	1071.02
	-2.80484
	1071.02
	14.40641
	1071.02
	-98.4769
	1071.02
	-37.4545

	1071.06
	24.76
	1071.69
	-25.0293
	1071.7
	-0.61265
	1071.7
	2.79304
	1071.7
	-3.51714
	1071.7
	14.51916
	1071.7
	-98.9946
	1071.7
	-36.373

	1071.75
	24.74383
	1072.38
	-26.5177
	1072.39
	1.85568
	1072.39
	3.13145
	1072.39
	-2.65622
	1072.39
	14.65629
	1072.39
	-97.9362
	1072.39
	-34.0216

	1072.44
	24.72727
	1073.07
	-27.2303
	1073.08
	1.89555
	1073.08
	4.4308
	1073.08
	-2.01888
	1073.08
	15.75434
	1073.08
	-97.1014
	1073.08
	-33.8606

	1073.13
	24.71034
	1073.75
	-28.4951
	1073.77
	1.90024
	1073.77
	6.72062
	1073.77
	-2.09078
	1073.77
	17.84287
	1073.77
	-96.9758
	1073.77
	-33.7347

	1073.82
	24.69298
	1073.97
	-29.559
	1074.46
	0.26709
	1074.46
	6.89599
	1074.46
	-1.70719
	1074.46
	17.81695
	1074.46
	-96.3948
	1074.46
	-35.2467

	1074.51
	24.67549
	1074.66
	-27.5866
	1075.15
	0.04236
	1075.15
	6.75986
	1075.15
	-0.89439
	1075.15
	17.47953
	1075.15
	-95.3845
	1075.15
	-35.3503

	1075.2
	24.65727
	1075.35
	-25.8006
	1075.84
	-1.08295
	1075.84
	9.78452
	1075.84
	1.54684
	1075.84
	20.3029
	1075.84
	-92.7458
	1075.84
	-36.3544

	1075.89
	24.63845
	1076.04
	-26.4299
	1076.53
	-2.03638
	1076.53
	11.40075
	1076.53
	4.55353
	1076.53
	21.71784
	1076.53
	-89.5417
	1076.53
	-37.1866

	1076.58
	24.6193
	1076.73
	-27.4793
	1077.22
	-1.84961
	1077.22
	11.17268
	1077.22
	6.72787
	1077.22
	21.28848
	1077.22
	-87.1699
	1077.22
	-36.8787

	1077.27
	24.60015
	1077.42
	-26.0357
	1077.91
	-0.74403
	1077.91
	12.23147
	1077.91
	8.35142
	1077.91
	22.14597
	1077.91
	-85.3489
	1077.91
	-35.6519

	1077.96
	24.58109
	1078.11
	-26.5846
	1078.6
	0.08999
	1078.6
	12.65653
	1078.6
	11.83183
	1078.6
	22.36974
	1078.6
	-81.671
	1078.6
	-34.6967

	1078.65
	24.56157
	1078.81
	-27.4993
	1079.29
	-0.00509
	1079.29
	14.16259
	1079.29
	13.04985
	1079.29
	23.67451
	1079.29
	-80.2555
	1079.29
	-34.6706

	1079.33
	24.54164
	1079.49
	-26.9383
	1079.97
	2.07629
	1079.97
	14.72671
	1079.97
	13.49015
	1079.97
	24.04026
	1079.97
	-79.6206
	1079.97
	-32.4698

	1080.02
	24.52104
	1080.19
	-29.98
	1080.66
	2.45133
	1080.66
	15.7069
	1080.66
	16.43186
	1080.66
	24.81916
	1080.66
	-76.4814
	1080.66
	-31.9736

	1080.71
	24.49932
	1080.88
	-29.2963
	1081.35
	2.28029
	1081.35
	18.082
	1081.35
	18.99122
	1081.35
	26.99297
	1081.35
	-73.7246
	1081.35
	-32.0235

	1081.4
	24.47652
	1081.57
	-27.8596
	1082.04
	2.37779
	1082.04
	19.36907
	1082.04
	21.56133
	1082.04
	28.07875
	1082.04
	-70.957
	1082.04
	-31.8048

	1082.09
	24.45237
	1082.26
	-28.9482
	1082.73
	3.00255
	1082.73
	19.50634
	1082.73
	24.73967
	1082.73
	28.01473
	1082.73
	-67.5812
	1082.73
	-31.0589

	1082.78
	24.42699
	1082.95
	-29.1091
	1083.42
	3.34997
	1083.42
	19.73205
	1083.42
	27.60367
	1083.42
	28.03915
	1083.42
	-64.5198
	1083.42
	-30.5903

	1083.47
	24.40005
	1083.64
	-28.7875
	1084.11
	3.70445
	1084.11
	21.5213
	1084.11
	29.67727
	1084.11
	29.6271
	1084.11
	-62.2487
	1084.11
	-30.1146

	1084.16
	24.37155
	1084.33
	-28.9286
	1084.79
	3.6552
	1084.79
	22.22135
	1084.79
	31.13354
	1084.79
	30.12878
	1084.79
	-60.5979
	1084.79
	-30.0445

	1084.85
	24.3417
	1085.02
	-31.7897
	1085.48
	5.24195
	1085.48
	24.49336
	1085.48
	32.62318
	1085.48
	32.1995
	1085.48
	-58.9107
	1085.48
	-28.3365

	1085.54
	24.31038
	1085.71
	-29.8496
	1086.17
	7.82753
	1086.17
	27.30988
	1086.17
	33.19282
	1086.17
	34.81473
	1086.17
	-58.1436
	1086.17
	-25.6298

	1086.23
	24.27764
	1086.4
	-31.2763
	1086.86
	10.3733
	1086.86
	29.21443
	1086.86
	34.92305
	1086.86
	36.51799
	1086.86
	-56.2159
	1086.86
	-22.9628

	1086.91
	24.2432
	1087.09
	-32.1213
	1087.55
	12.2786
	1087.55
	30.18881
	1087.55
	37.58207
	1087.55
	37.29108
	1087.55
	-53.3595
	1087.55
	-20.9363

	1087.6
	24.20676
	1087.78
	-30.5206
	1088.23
	10.54232
	1088.23
	32.04556
	1088.23
	39.64022
	1088.23
	38.94946
	1088.23
	-51.1067
	1088.23
	-22.5532

	1088.29
	24.16839
	1088.46
	-32.4614
	1088.92
	12.82488
	1088.92
	34.03268
	1088.92
	40.55081
	1088.92
	40.73529
	1088.92
	-49.9987
	1088.92
	-20.1495

	1088.98
	24.12758
	1089.15
	-31.9223
	1089.61
	13.80449
	1089.61
	34.73628
	1089.61
	42.83395
	1089.61
	41.23759
	1089.61
	-47.5181
	1089.61
	-19.0487

	1089.67
	24.08418
	1089.84
	-31.3774
	1090.3
	14.33018
	1090.3
	37.18673
	1090.3
	43.73042
	1090.3
	43.48675
	1090.3
	-46.4241
	1090.3
	-18.4018

	1090.36
	24.03796
	1090.53
	-32.6259
	1090.98
	14.41775
	1090.98
	37.27938
	1090.98
	44.89089
	1090.98
	43.38103
	1090.98
	-45.0691
	1090.98
	-18.1948

	1091.05
	23.9889
	1091.22
	-33.4974
	1091.67
	16.1761
	1091.67
	37.05377
	1091.67
	46.24105
	1091.67
	42.95413
	1091.67
	-43.5214
	1091.67
	-16.3153

	1091.73
	23.93713
	1091.91
	-34.2218
	1092.36
	17.07438
	1092.36
	37.52681
	1092.36
	47.92568
	1092.36
	43.22588
	1092.36
	-41.6393
	1092.36
	-15.2958

	1092.42
	23.88243
	1092.6
	-33.6778
	1093.05
	19.23324
	1093.05
	38.11651
	1093.05
	49.36188
	1093.05
	43.61429
	1093.05
	-40.0057
	1093.05
	-13.0158

	1093.11
	23.8243
	1093.29
	-33.4922
	1093.73
	18.25229
	1093.73
	38.78644
	1093.73
	51.28055
	1093.73
	44.08584
	1093.73
	-37.8924
	1093.73
	-13.8773

	1093.8
	23.76198
	1093.98
	-32.7792
	1094.42
	18.69245
	1094.42
	38.98184
	1094.42
	51.70063
	1094.42
	44.07995
	1094.42
	-37.2749
	1094.42
	-13.316

	1094.49
	23.69501
	1094.67
	-31.2363
	1095.11
	18.79907
	1095.11
	39.46176
	1095.11
	53.76719
	1095.11
	44.35858
	1095.11
	-35.0108
	1095.11
	-13.0882

	1095.17
	23.62291
	1095.36
	-32.2796
	1095.8
	21.10013
	1095.8
	40.07404
	1095.8
	55.47861
	1095.8
	44.76957
	1095.8
	-33.102
	1095.8
	-10.666

	1095.86
	23.54583
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	-45.4873
	1118.43
	4.01389

	1118.52
	17.6029
	1118.73
	-31.7105
	1119.12
	31.33724
	1119.12
	42.28698
	1119.12
	36.03454
	1119.12
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	1124.69
	15.15311
	1124.91
	-28.2453
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	1131.43
	24.59075
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	13.91275
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	12.35862
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	12.26085
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	7.43379
	1205.15
	27.52993
	1205.15
	32.72768
	1205.15
	37.29923
	1205.15
	-39.963
	1205.15
	-4.17203

	1205.71
	-5.66974
	1206.04
	-41.7312
	1205.83
	8.06884
	1205.83
	26.91354
	1205.83
	32.76531
	1205.83
	36.7426
	1205.83
	-40.2197
	1205.83
	-3.39631

	1206.39
	-5.72326
	1206.72
	-41.1106
	1206.5
	7.6299
	1206.5
	26.90495
	1206.5
	32.62067
	1206.5
	36.79289
	1206.5
	-40.6543
	1206.5
	-3.69663

	1207.07
	-5.77743
	1207.4
	-39.8336
	1207.18
	7.97208
	1207.18
	26.7413
	1207.18
	33.6233
	1207.18
	36.689
	1207.18
	-39.946
	1207.18
	-3.21378

	1207.74
	-5.83212
	1208.07
	-40.6893
	1207.86
	9.43528
	1207.86
	25.45954
	1207.86
	34.52749
	1207.86
	35.46701
	1207.86
	-39.3361
	1207.86
	-1.60989

	1208.42
	-5.88723
	1208.75
	-40.1641
	1208.54
	8.87537
	1208.54
	25.48059
	1208.54
	33.55687
	1208.54
	35.54781
	1208.54
	-40.6011
	1208.54
	-2.02912

	1209.1
	-5.94247
	1209.43
	-41.5469
	1209.21
	7.99699
	1209.21
	25.58617
	1209.21
	34.18663
	1209.21
	35.71228
	1209.21
	-40.2613
	1209.21
	-2.7689

	1209.77
	-5.99805
	1210.11
	-42.9416
	1209.89
	7.52574
	1209.89
	25.79309
	1209.89
	36.0567
	1209.89
	35.97896
	1209.89
	-38.6856
	1209.89
	-3.09947

	1210.45
	-6.05409
	1210.78
	-43.2261
	1210.57
	7.51056
	1210.57
	25.03995
	1210.57
	33.52695
	1210.57
	35.28558
	1210.57
	-41.5097
	1210.57
	-2.97397

	1211.13
	-6.11091
	1211.46
	-43.6736
	1211.25
	7.15401
	1211.25
	23.08929
	1211.25
	33.56623
	1211.25
	33.39468
	1211.25
	-41.7647
	1211.25
	-3.18984

	1211.8
	-6.16829
	1212.14
	-43.4366
	1211.93
	6.30176
	1211.93
	22.51516
	1211.93
	32.92697
	1211.93
	32.88031
	1211.93
	-42.6983
	1211.93
	-3.90141

	1212.48
	-6.22634
	1212.82
	-43.1148
	1212.6
	6.84452
	1212.6
	22.03438
	1212.6
	33.93436
	1212.6
	32.45842
	1212.6
	-41.9809
	1212.6
	-3.22004

	1213.15
	-6.28498
	1213.49
	-43.4355
	1213.28
	6.95284
	1213.28
	21.66142
	1213.28
	35.525
	1213.28
	32.14521
	1213.28
	-40.6846
	1213.28
	-2.97105

	1213.83
	-6.34399
	1214.17
	-46.1328
	1213.96
	7.38723
	1213.96
	20.65584
	1213.96
	35.92465
	1213.96
	31.19939
	1213.96
	-40.5793
	1213.96
	-2.39597

	1214.51
	-6.40316
	1214.85
	-46.8639
	1214.63
	8.0486
	1214.63
	20.91294
	1214.63
	36.17802
	1214.63
	31.51538
	1214.63
	-40.6159
	1214.63
	-1.59599

	1215.18
	-6.46219
	1215.52
	-47.2546
	1215.31
	9.75868
	1215.31
	21.22381
	1215.31
	36.58257
	1215.31
	31.886
	1215.31
	-40.5057
	1215.31
	0.25477

	1215.86
	-6.52095
	1216.2
	-47.009
	1215.99
	11.12543
	1215.99
	22.5599
	1215.99
	36.07026
	1215.99
	33.28186
	1215.99
	-41.3123
	1215.99
	1.76219

	1216.53
	-6.5788
	1216.88
	-45.2967
	1216.67
	12.58432
	1216.67
	22.26279
	1216.67
	36.52609
	1216.67
	33.0445
	1216.67
	-41.1508
	1216.67
	3.36176

	1217.21
	-6.63605
	1217.55
	-44.2372
	1217.34
	12.86763
	1217.34
	22.40322
	1217.34
	33.71542
	1217.34
	33.24381
	1217.34
	-44.2515
	1217.34
	3.78368

	1217.88
	-6.6927
	1218.23
	-44.3459
	1218.02
	13.27121
	1218.02
	21.44465
	1218.02
	33.2082
	1218.02
	32.34501
	1218.02
	-45.053
	1218.02
	4.32794

	1218.56
	-6.74835
	1218.91
	-45.1936
	1218.7
	13.1391
	1218.7
	21.38119
	1218.7
	30.56764
	1218.7
	32.34131
	1218.7
	-47.9879
	1218.7
	4.3365

	1219.23
	-6.80292
	1219.58
	-45.3452
	1219.37
	13.66747
	1219.37
	20.92284
	1219.37
	28.78794
	1219.37
	31.94184
	1219.37
	-50.0576
	1219.37
	5.00349

	1219.91
	-6.8561
	1220.26
	-46.0294
	1220.05
	13.44203
	1220.05
	19.49525
	1220.05
	27.34385
	1220.05
	30.57402
	1220.05
	-51.796
	1220.05
	4.91872

	1220.59
	-6.90764
	1220.94
	-45.8693
	1220.73
	14.26147
	1220.73
	16.57367
	1220.73
	25.96378
	1220.73
	27.7122
	1220.73
	-53.4704
	1220.73
	5.87884

	1221.26
	-6.95718
	1221.61
	-44.6303
	1221.4
	15.41847
	1221.4
	17.9114
	1221.4
	24.99839
	1221.4
	29.10881
	1221.4
	-54.7258
	1221.4
	7.17445

	1221.94
	-7.00443
	1222.29
	-44.7701
	1222.08
	16.7722
	1222.08
	18.16877
	1222.08
	25.46978
	1222.08
	29.42593
	1222.08
	-54.5487
	1222.08
	8.66887

	1222.61
	-7.04885
	1222.96
	-45.5768
	1222.76
	16.02849
	1222.76
	18.0375
	1222.76
	23.08705
	1222.76
	29.35443
	1222.76
	-57.2258
	1222.76
	8.06583

	1223.29
	-7.09057
	1223.64
	-48.1652
	1223.43
	15.9182
	1223.43
	18.56744
	1223.43
	23.58714
	1223.43
	29.94324
	1223.43
	-57.0157
	1223.43
	8.09415

	1223.96
	-7.12922
	1224.32
	-48.5196
	1224.11
	16.2788
	1224.11
	18.64872
	1224.11
	24.01931
	1224.11
	30.08429
	1224.11
	-56.8779
	1224.11
	8.59543

	1224.64
	-7.16458
	1224.99
	-48.7012
	1224.79
	17.08212
	1224.79
	18.57699
	1224.79
	24.58294
	1224.79
	30.07232
	1224.79
	-56.6086
	1224.79
	9.53943

	1225.31
	-7.19644
	1225.67
	-49.1757
	1225.46
	18.1573
	1225.46
	18.87175
	1225.46
	24.32626
	1225.46
	30.42596
	1225.46
	-57.1552
	1225.46
	10.75322

	1225.99
	-7.22436
	1226.34
	-48.8293
	1226.14
	18.87826
	1226.14
	19.38112
	1226.14
	24.52626
	1226.14
	30.99509
	1226.14
	-57.2496
	1226.14
	11.61485

	1226.66
	-7.24841
	1227.02
	-48.9513
	1226.81
	17.59109
	1226.81
	18.89333
	1226.81
	23.82879
	1226.81
	30.56619
	1226.81
	-58.237
	1226.81
	10.46629

	1227.34
	-7.26866
	1227.7
	-50.2235
	1227.49
	15.93792
	1227.49
	17.61624
	1227.49
	23.15487
	1227.49
	29.34885
	1227.49
	-59.2053
	1227.49
	8.95381

	1228.01
	-7.2848
	1228.37
	-50.229
	1228.17
	17.00631
	1228.17
	17.43494
	1228.17
	23.63751
	1228.17
	29.22732
	1228.17
	-59.017
	1228.17
	10.16288

	1228.68
	-7.29673
	1229.05
	-50.8249
	1228.84
	18.29814
	1228.84
	14.35767
	1228.84
	22.3768
	1228.84
	26.20892
	1228.84
	-60.5677
	1228.84
	11.59332

	1229.36
	-7.30418
	1229.72
	-51.0746
	1229.52
	18.03063
	1229.52
	13.64709
	1229.52
	21.95364
	1229.52
	25.5581
	1229.52
	-61.2852
	1229.52
	11.46648

	1230.03
	-7.30743
	1230.4
	-49.4591
	1230.19
	17.85342
	1230.19
	11.91993
	1230.19
	24.63518
	1230.19
	23.88983
	1230.19
	-58.8936
	1230.19
	11.42788

	1230.71
	-7.30658
	1231.07
	-47.4189
	1230.87
	17.31473
	1230.87
	12.20562
	1230.87
	24.41614
	1230.87
	24.23528
	1230.87
	-59.407
	1230.87
	11.02987

	1231.38
	-7.30153
	1231.75
	-48.0457
	1231.54
	17.1677
	1231.54
	12.70898
	1231.54
	24.0911
	1231.54
	24.79752
	1231.54
	-60.022
	1231.54
	11.02145

	1232.06
	-7.29251
	1232.42
	-48.2471
	1232.22
	15.03568
	1232.22
	11.07565
	1232.22
	23.11187
	1232.22
	23.22396
	1232.22
	-61.2956
	1232.22
	9.03011

	1232.73
	-7.27952
	1233.1
	-48.3597
	1232.9
	16.22639
	1232.9
	11.3746
	1232.9
	23.46194
	1232.9
	23.58267
	1232.9
	-61.2398
	1232.9
	10.36149

	1233.41
	-7.26249
	1233.77
	-48.5684
	1233.57
	16.88659
	1233.57
	9.12808
	1233.57
	22.54032
	1233.57
	21.39503
	1233.57
	-62.4515
	1233.57
	11.16031

	1234.08
	-7.24151
	1234.45
	-48.5067
	1234.25
	18.00865
	1234.25
	9.70716
	1234.25
	21.81264
	1234.25
	22.03386
	1234.25
	-63.4735
	1234.25
	12.42305

	1234.75
	-7.21643
	1235.12
	-48.2426
	1234.92
	16.79494
	1234.92
	10.41083
	1234.92
	19.32848
	1234.92
	22.79642
	1234.92
	-66.2476
	1234.92
	11.34794

	1235.43
	-7.18701
	1235.8
	-49.7289
	1235.6
	17.22345
	1235.6
	10.76944
	1235.6
	18.39893
	1235.6
	23.21478
	1235.6
	-67.4715
	1235.6
	11.91714

	1236.1
	-7.15303
	1236.47
	-49.607
	1236.27
	18.77972
	1236.27
	10.37539
	1236.27
	20.20877
	1236.27
	22.87962
	1236.27
	-65.9517
	1236.27
	13.61201

	1236.77
	-7.11478
	1237.15
	-50.9048
	1236.95
	19.22098
	1236.95
	11.23164
	1236.95
	20.22197
	1236.95
	23.79563
	1236.95
	-66.2328
	1236.95
	14.19395

	1237.45
	-7.07263
	1237.82
	-51.554
	1237.62
	19.2635
	1237.62
	11.7834
	1237.62
	21.45661
	1237.62
	24.40627
	1237.62
	-65.2882
	1237.62
	14.37508

	1238.12
	-7.0271
	1238.5
	-52.3152
	1238.3
	20.85905
	1238.3
	12.60958
	1238.3
	22.90989
	1238.3
	25.29221
	1238.3
	-64.1292
	1238.3
	16.11131

	1238.8
	-6.97873
	1239.17
	-52.3763
	1238.97
	19.74981
	1238.97
	12.08703
	1238.97
	20.10414
	1238.97
	24.82854
	1238.97
	-67.2249
	1238.97
	15.14068

	1239.47
	-6.92777
	1239.85
	-52.7739
	1239.65
	19.42437
	1239.65
	11.51627
	1239.65
	19.7832
	1239.65
	24.31754
	1239.65
	-67.8402
	1239.65
	14.95592

	1240.14
	-6.87462
	1240.52
	-53.0328
	1240.32
	19.34491
	1240.32
	11.72266
	1240.32
	19.54264
	1240.32
	24.58281
	1240.32
	-68.3708
	1240.32
	15.01507

	1240.82
	-6.82009
	1241.19
	-52.9161
	1241
	19.54927
	1241
	11.19131
	1241
	18.92915
	1241
	24.11123
	1241
	-69.2786
	1241
	15.36011

	1241.49
	-6.76423
	1241.87
	-53.6051
	1241.67
	20.11293
	1241.67
	10.66351
	1241.67
	17.90535
	1241.67
	23.64231
	1241.67
	-70.5924
	1241.67
	16.06238

	1242.16
	-6.70719
	1242.54
	-54.2888
	1242.34
	18.75111
	1242.34
	9.95139
	1242.34
	17.98566
	1242.34
	22.98908
	1242.34
	-70.8021
	1242.34
	14.83917

	1242.84
	-6.64925
	1243.22
	-53.1116
	1243.02
	18.88663
	1243.02
	9.24409
	1243.02
	18.9454
	1243.02
	22.34153
	1243.02
	-70.1367
	1243.02
	15.11536

	1243.51
	-6.59056
	1243.89
	-52.918
	1243.69
	20.32596
	1243.69
	8.57347
	1243.69
	18.26129
	1243.69
	21.72979
	1243.69
	-71.1108
	1243.69
	16.69331

	1244.18
	-6.53154
	1244.56
	-51.3711
	1244.37
	19.4746
	1244.37
	6.03491
	1244.37
	17.33603
	1244.37
	19.25099
	1244.37
	-72.3304
	1244.37
	15.98262

	1244.85
	-6.4727
	1245.24
	-51.8825
	1245.04
	19.92412
	1245.04
	5.32292
	1245.04
	17.03525
	1245.04
	18.59788
	1245.04
	-72.9211
	1245.04
	16.57076

	1245.53
	-6.41457
	1245.91
	-52.2876
	1245.72
	20.15039
	1245.72
	5.79997
	1245.72
	16.21811
	1245.72
	19.1347
	1245.72
	-74.0326
	1245.72
	16.9377

	1246.2
	-6.3575
	1246.59
	-52.4244
	1246.39
	19.68853
	1246.39
	5.11418
	1246.39
	13.91959
	1246.39
	18.50778
	1246.39
	-76.6211
	1246.39
	16.61445

	1246.87
	-6.30151
	1247.26
	-52.7324
	1247.06
	18.07645
	1247.06
	5.80654
	1247.06
	14.28801
	1247.06
	19.25903
	1247.06
	-76.5427
	1247.06
	15.14099

	1247.55
	-6.24692
	1247.93
	-51.8862
	1247.74
	17.76742
	1247.74
	5.20379
	1247.74
	11.71577
	1247.74
	18.71604
	1247.74
	-79.4093
	1247.74
	14.97264

	1248.22
	-6.19378
	1248.61
	-51.3059
	1248.41
	16.68025
	1248.41
	4.28832
	1248.41
	12.36871
	1248.41
	17.85945
	1248.41
	-79.0463
	1248.41
	14.02407

	1248.89
	-6.14226
	1249.28
	-51.0635
	1249.09
	16.29767
	1249.09
	3.98216
	1249.09
	10.79303
	1249.09
	17.61305
	1249.09
	-80.9163
	1249.09
	13.78217

	1249.56
	-6.09249
	1249.95
	-50.0768
	1249.76
	14.87597
	1249.76
	2.11484
	1249.76
	7.14743
	1249.76
	15.80462
	1249.76
	-84.8519
	1249.76
	12.49908

	1250.24
	-6.04463
	1250.63
	-50.9886
	1250.43
	12.88582
	1250.43
	0.82137
	1250.43
	5.61545
	1250.43
	14.57003
	1250.43
	-86.6739
	1250.43
	10.64754

	1250.91
	-5.99892
	1251.3
	-51.6733
	1251.11
	11.31558
	1251.11
	0.97985
	1251.11
	3.83437
	1251.11
	14.78826
	1251.11
	-88.7493
	1251.11
	9.21798

	1251.58
	-5.95533
	1251.97
	-52.5615
	1251.78
	10.79935
	1251.78
	0.24442
	1251.78
	4.4971
	1251.78
	14.11172
	1251.78
	-88.3766
	1251.78
	8.84036

	1252.25
	-5.91452
	1252.65
	-54.5117
	1252.45
	10.6494
	1252.45
	-1.23729
	1252.45
	1.94178
	1252.45
	12.68889
	1252.45
	-91.2219
	1252.45
	8.82901

	1252.93
	-5.87678
	1253.32
	-54.5323
	1253.13
	9.53814
	1253.13
	-1.07857
	1253.13
	2.55265
	1253.13
	12.90737
	1253.13
	-90.9054
	1253.13
	7.85843

	1253.6
	-5.84193
	1253.99
	-54.967
	1253.8
	10.58071
	1253.8
	-1.20918
	1253.8
	3.16958
	1253.8
	12.83565
	1253.8
	-90.5784
	1253.8
	9.03962

	1254.27
	-5.81033
	1254.67
	-56.0959
	1254.47
	11.12386
	1254.47
	0.08339
	1254.47
	1.91327
	1254.47
	14.19169
	1254.47
	-92.1247
	1254.47
	9.72138

	1254.94
	-5.78225
	1255.34
	-55.7728
	1255.15
	10.59456
	1255.15
	0.65056
	1255.15
	0.85257
	1255.15
	14.88742
	1255.15
	-93.4798
	1255.15
	9.33276

	1255.61
	-5.75795
	1256.01
	-56.9134
	1255.82
	9.3581
	1255.82
	0.07779
	1255.82
	2.63548
	1255.82
	14.44131
	1255.82
	-91.9869
	1255.82
	8.23491

	1256.29
	-5.73726
	1256.68
	-56.3015
	1256.49
	10.12184
	1256.49
	0.36462
	1256.49
	1.3523
	1256.49
	14.85481
	1256.49
	-93.56
	1256.49
	9.13725

	1256.96
	-5.72
	1257.36
	-56.7109
	1257.17
	9.10741
	1257.17
	-0.09503
	1257.17
	0.91884
	1257.17
	14.52373
	1257.17
	-94.2878
	1257.17
	8.2635

	1257.63
	-5.70588
	1258.03
	-55.4693
	1257.84
	9.93544
	1257.84
	-0.56082
	1257.84
	-1.11973
	1257.84
	14.1846
	1257.84
	-96.6164
	1257.84
	9.23014

	1258.3
	-5.69494
	1258.7
	-56.5302
	1258.51
	7.98541
	1258.51
	-0.98728
	1258.51
	-1.38253
	1258.51
	13.88481
	1258.51
	-97.1692
	1258.51
	7.41872

	1258.97
	-5.68708
	1259.38
	-56.9574
	1259.19
	6.03135
	1259.19
	-0.36582
	1259.19
	-2.23492
	1259.19
	14.63483
	1259.19
	-98.3159
	1259.19
	5.60534

	1259.64
	-5.68217
	1260.05
	-54.5287
	1259.86
	6.12115
	1259.86
	1.68545
	1259.86
	-2.11859
	1259.86
	16.81276
	1259.86
	-98.4896
	1259.86
	5.83375

	1260.31
	-5.68013
	1260.72
	-53.7584
	1260.53
	5.94093
	1260.53
	0.97997
	1260.53
	0.4839
	1260.53
	16.23395
	1260.53
	-96.1771
	1260.53
	5.79214

	1260.99
	-5.68052
	1261.39
	-53.5631
	1261.2
	6.0856
	1261.2
	1.67744
	1261.2
	-0.84046
	1261.2
	17.05808
	1261.2
	-97.7914
	1261.2
	6.07543

	1261.66
	-5.6833
	1262.06
	-51.6519
	1261.88
	6.808
	1261.88
	2.8147
	1261.88
	0.51841
	1261.88
	18.32391
	1261.88
	-96.7269
	1261.88
	6.9385

	1262.33
	-5.68852
	1262.74
	-52.3371
	1262.55
	7.74737
	1262.55
	4.35935
	1262.55
	-0.47822
	1262.55
	19.99522
	1262.55
	-98.0135
	1262.55
	8.01648

	1263
	-5.69626
	1263.41
	-53.4342
	1263.22
	7.92711
	1263.22
	4.98294
	1263.22
	1.11079
	1263.22
	20.74548
	1263.22
	-96.3134
	1263.22
	8.33483

	1263.67
	-5.70655
	1264.08
	-54.5436
	1263.89
	7.79528
	1263.89
	4.35064
	1263.89
	1.65135
	1263.89
	20.23985
	1263.89
	-95.5348
	1263.89
	8.34161

	1264.34
	-5.71914
	1264.75
	-54.1229
	1264.57
	7.22138
	1264.57
	6.03019
	1264.57
	-0.4636
	1264.57
	22.04795
	1264.57
	-97.4082
	1264.57
	7.90839

	1265.01
	-5.73371
	1265.42
	-54.73
	1265.24
	6.4515
	1265.24
	6.01017
	1265.24
	0.08215
	1265.24
	22.1546
	1265.24
	-96.6245
	1265.24
	7.27712

	1265.68
	-5.75023
	1266.1
	-53.7197
	1265.91
	6.3724
	1265.91
	7.69643
	1265.91
	0.65026
	1265.91
	23.96753
	1265.91
	-95.8184
	1265.91
	7.33663

	1266.35
	-5.76844
	1266.77
	-53.4825
	1266.58
	7.18367
	1266.58
	8.09281
	1266.58
	3.06257
	1266.58
	24.49058
	1266.58
	-93.1681
	1266.58
	8.28651

	1267.03
	-5.78802
	1267.44
	-52.7296
	1267.25
	5.81259
	1267.25
	8.76115
	1267.25
	1.83312
	1267.25
	25.28559
	1267.25
	-94.1595
	1267.25
	7.05404

	1267.7
	-5.80882
	1268.11
	-53.8642
	1267.93
	6.39356
	1267.93
	11.39525
	1267.93
	2.856
	1267.93
	28.04825
	1267.93
	-92.8951
	1267.93
	7.77569

	1268.37
	-5.83066
	1268.78
	-54.5532
	1268.6
	5.64756
	1268.6
	10.52744
	1268.6
	2.36742
	1268.6
	27.3071
	1268.6
	-93.1457
	1268.6
	7.1683

	1269.04
	-5.85327
	1269.45
	-55.5738
	1269.27
	8.33784
	1269.27
	11.73669
	1269.27
	3.26335
	1269.27
	28.64302
	1269.27
	-92.0118
	1269.27
	9.99718

	1269.71
	-5.8768
	1270.13
	-56.0728
	1269.94
	7.8038
	1269.94
	11.69751
	1269.94
	3.51046
	1269.94
	28.7305
	1269.94
	-91.5267
	1269.94
	9.60176

	1270.38
	-5.90122
	1270.8
	-55.203
	1270.61
	7.19661
	1270.61
	12.45021
	1270.61
	2.96707
	1270.61
	29.60987
	1270.61
	-91.832
	1270.61
	9.13317

	1271.05
	-5.92628
	1271.47
	-57.2667
	1271.28
	8.06118
	1271.28
	12.87781
	1271.28
	2.51035
	1271.28
	30.16414
	1271.28
	-92.0508
	1271.28
	10.13635

	1271.72
	-5.95203
	1272.14
	-58.4404
	1271.96
	7.16878
	1271.96
	13.97804
	1271.96
	1.63184
	1271.96
	31.39292
	1271.96
	-92.6877
	1271.96
	9.38463

	1272.39
	-5.97807
	1272.81
	-59.0732
	1272.63
	5.66431
	1272.63
	12.94635
	1272.63
	1.7354
	1272.63
	30.4879
	1272.63
	-92.3462
	1272.63
	8.01878

	1273.06
	-6.00419
	1273.48
	-59.5242
	1273.3
	5.35318
	1273.3
	13.93721
	1273.3
	4.39896
	1273.3
	31.60543
	1273.3
	-89.4446
	1273.3
	7.84625

	1273.73
	-6.03045
	1274.15
	-59.6179
	1273.97
	5.17126
	1273.97
	16.21905
	1273.97
	3.20037
	1273.97
	34.01394
	1273.97
	-90.4052
	1273.97
	7.80294

	1274.4
	-6.05664
	1274.82
	-61.5054
	1274.64
	4.89011
	1274.64
	16.79612
	1274.64
	2.94324
	1274.64
	34.71767
	1274.64
	-90.4243
	1274.64
	7.6604

	1275.07
	-6.0828
	1275.49
	-61.449
	1275.31
	4.74014
	1275.31
	15.99553
	1275.31
	4.4316
	1275.31
	34.04376
	1275.31
	-88.698
	1275.31
	7.64904

	1275.74
	-6.1091
	1276.17
	-60.7226
	1275.98
	3.68604
	1275.98
	15.62142
	1275.98
	4.09035
	1275.98
	33.79631
	1275.98
	-88.8012
	1275.98
	6.73356

	1276.41
	-6.13345
	1276.84
	-61.2627
	1276.66
	5.1583
	1276.66
	15.6922
	1276.66
	5.52995
	1276.66
	33.99565
	1276.66
	-87.1201
	1276.66
	8.34649

	1277.08
	-6.15573
	1277.51
	-61.0864
	1277.33
	4.09732
	1277.33
	17.31546
	1277.33
	6.82683
	1277.33
	35.74558
	1277.33
	-85.5852
	1277.33
	7.42412

	1277.75
	-6.17604
	1278.18
	-60.6989
	1278
	3.78027
	1278
	17.66637
	1278
	7.86371
	1278
	36.22315
	1278
	-84.3103
	1278
	7.24568

	1278.42
	-6.19415
	1278.85
	-59.3811
	1278.67
	6.28891
	1278.67
	19.48845
	1278.67
	7.20373
	1278.67
	38.17191
	1278.67
	-84.7323
	1278.67
	9.89293

	1279.09
	-6.21007
	1279.52
	-58.3815
	1279.34
	5.49713
	1279.34
	21.64125
	1279.34
	7.81776
	1279.34
	40.45137
	1279.34
	-83.8803
	1279.34
	9.23976

	1279.76
	-6.22363
	1280.19
	-58.8889
	1280.01
	6.89281
	1280.01
	22.58345
	1280.01
	9.30708
	1280.01
	41.52024
	1280.01
	-82.153
	1280.01
	10.77405

	1280.43
	-6.23499
	1280.86
	-58.5205
	1280.68
	8.20162
	1280.68
	22.5986
	1280.68
	11.57386
	1280.68
	41.66206
	1280.68
	-79.6482
	1280.68
	12.22147

	1281.1
	-6.2443
	1281.53
	-57.9997
	1281.35
	10.06749
	1281.35
	22.97395
	1281.35
	12.73867
	1281.35
	42.16407
	1281.35
	-78.2454
	1281.35
	14.22595

	1281.77
	-6.25135
	1282.2
	-58.0616
	1282.02
	11.79609
	1282.02
	23.17392
	1282.02
	14.9171
	1282.02
	42.49071
	1282.02
	-75.829
	1282.02
	16.09316

	1282.43
	-6.25592
	1282.87
	-57.7463
	1282.69
	13.16957
	1282.69
	25.69421
	1282.69
	14.53661
	1282.69
	45.13767
	1282.69
	-75.9715
	1282.69
	17.60525

	1283.1
	-6.25785
	1283.54
	-58.8464
	1283.36
	14.37619
	1283.36
	26.8945
	1283.36
	16.07866
	1283.36
	46.46463
	1283.36
	-74.1914
	1283.36
	18.95048

	1283.77
	-6.25727
	1284.21
	-57.8155
	1284.03
	14.49124
	1284.03
	29.15225
	1284.03
	17.63346
	1284.03
	48.84904
	1284.03
	-72.3986
	1284.03
	19.20414

	1284.44
	-6.25415
	1284.88
	-57.823
	1284.7
	15.51355
	1284.7
	30.82077
	1284.7
	19.47532
	1284.7
	50.64423
	1284.7
	-70.3188
	1284.7
	20.36506

	1285.11
	-6.24845
	1285.55
	-59.16
	1285.37
	16.54721
	1285.37
	32.48903
	1285.37
	22.20158
	1285.37
	52.43915
	1285.37
	-67.3545
	1285.37
	21.53733

	1285.78
	-6.24026
	1286.22
	-59.1194
	1286.04
	17.73832
	1286.04
	33.72728
	1286.04
	23.84666
	1286.04
	53.80408
	1286.04
	-65.4714
	1286.04
	22.86705

	1286.45
	-6.22971
	1286.89
	-61.1275
	1286.71
	17.46981
	1286.71
	34.96468
	1286.71
	26.57615
	1286.71
	55.16814
	1286.71
	-62.5039
	1286.71
	22.73715

	1287.12
	-6.217
	1287.56
	-60.0732
	1287.38
	18.23933
	1287.38
	36.57365
	1287.38
	28.47701
	1287.38
	56.90378
	1287.38
	-60.3651
	1287.38
	23.64528

	1287.79
	-6.2022
	1288.23
	-60.8466
	1288.05
	17.74455
	1288.05
	36.543
	1288.05
	30.38513
	1288.05
	56.9998
	1288.05
	-58.219
	1288.05
	23.2891

	1288.45
	-6.18491
	1288.9
	-61.6142
	1288.72
	17.48976
	1288.72
	36.24001
	1288.72
	30.5803
	1288.72
	56.82347
	1288.72
	-57.7858
	1288.72
	23.17292

	1289.12
	-6.16516
	1289.57
	-61.8156
	1289.39
	18.12142
	1289.39
	36.89537
	1289.39
	32.37106
	1289.39
	57.6055
	1289.39
	-55.757
	1289.39
	23.9432

	1289.79
	-6.14333
	1290.24
	-62.3306
	1290.06
	18.75328
	1290.06
	37.02779
	1290.06
	31.93475
	1290.06
	57.86459
	1290.06
	-55.9553
	1290.06
	24.71367

	1290.46
	-6.11958
	1290.91
	-61.3914
	1290.73
	16.81199
	1290.73
	37.62504
	1290.73
	32.27717
	1290.73
	58.5885
	1290.73
	-55.3749
	1290.73
	22.91098

	1291.13
	-6.09385
	1291.58
	-62.0566
	1291.4
	17.46618
	1291.4
	37.68444
	1291.4
	33.93193
	1291.4
	58.77457
	1291.4
	-53.4822
	1291.4
	23.70379

	1291.8
	-6.06622
	1292.25
	-63.0676
	1292.07
	17.8094
	1292.07
	38.14914
	1292.07
	34.14984
	1292.07
	59.36594
	1292.07
	-53.0263
	1292.07
	24.18561

	1292.46
	-6.03648
	1292.91
	-62.0768
	1292.74
	19.83045
	1292.74
	37.99462
	1292.74
	35.82519
	1292.74
	59.33809
	1292.74
	-51.1129
	1292.74
	26.34528

	1293.13
	-6.00459
	1293.58
	-61.9981
	1293.41
	23.36112
	1293.41
	37.81148
	1293.41
	35.56976
	1293.41
	59.28161
	1293.41
	-51.1303
	1293.41
	30.01455

	1293.8
	-5.97075
	1294.25
	-60.7358
	1294.08
	23.95626
	1294.08
	35.92759
	1294.08
	38.25804
	1294.08
	57.52439
	1294.08
	-48.2041
	1294.08
	30.7483

	1294.47
	-5.93501
	1294.92
	-61.7526
	1294.75
	25.06748
	1294.75
	37.20665
	1294.75
	36.6024
	1294.75
	58.93012
	1294.75
	-49.6217
	1294.75
	31.99813

	1295.14
	-5.8973
	1295.59
	-61.1351
	1295.42
	26.84752
	1295.42
	37.50904
	1295.42
	39.18637
	1295.42
	59.35918
	1295.42
	-46.7997
	1295.42
	33.91678

	1295.8
	-5.85775
	1296.26
	-60.5493
	1296.09
	28.33972
	1296.09
	37.22849
	1296.09
	40.67837
	1296.09
	59.20529
	1296.09
	-45.0697
	1296.09
	35.54759

	1296.47
	-5.81613
	1296.93
	-60.0982
	1296.76
	29.4219
	1296.76
	36.79924
	1296.76
	41.37576
	1296.76
	58.90271
	1296.76
	-44.1344
	1296.76
	36.76838

	1297.14
	-5.77234
	1297.6
	-59.8747
	1297.43
	30.07231
	1297.43
	37.19959
	1297.43
	40.96707
	1297.43
	59.42973
	1297.43
	-44.3051
	1297.43
	37.55741

	1297.81
	-5.72687
	1298.27
	-59.9946
	1298.1
	30.28488
	1298.1
	38.20681
	1298.1
	42.26329
	1298.1
	60.56362
	1298.1
	-42.7708
	1298.1
	37.90859

	1298.48
	-5.6801
	1298.93
	-60.3567
	1298.77
	31.03942
	1298.77
	38.26913
	1298.77
	43.67754
	1298.77
	60.7526
	1298.77
	-41.1186
	1298.77
	38.80173

	1299.14
	-5.63214
	1299.6
	-58.171
	1299.43
	33.73247
	1299.43
	39.62365
	1299.43
	44.64798
	1299.43
	62.2319
	1299.43
	-39.9137
	1299.43
	41.63133

	1299.81
	-5.58263
	1300.27
	-56.8034
	1300.1
	34.47503
	1300.1
	38.63432
	1300.1
	44.76487
	1300.1
	61.36924
	1300.1
	-39.5588
	1300.1
	42.51249

	1300.48
	-5.5316
	1300.94
	-56.2198
	1300.77
	35.38425
	1300.77
	39.46617
	1300.77
	43.42961
	1300.77
	62.32776
	1300.77
	-40.6561
	1300.77
	43.56032

	1301.15
	-5.47906
	1301.61
	-55.9657
	1301.44
	35.96188
	1301.44
	40.24285
	1301.44
	44.95424
	1301.44
	63.2311
	1301.44
	-38.8935
	1301.44
	44.27657

	1301.81
	-5.42481
	1302.28
	-55.2728
	1302.11
	35.38658
	1302.11
	40.40541
	1302.11
	45.50475
	1302.11
	63.52033
	1302.11
	-38.1049
	1302.11
	43.83987

	1302.48
	-5.36887
	1302.94
	-55.2152
	1302.78
	35.33107
	1302.78
	40.50777
	1302.78
	46.62291
	1302.78
	63.74936
	1302.78
	-36.7488
	1302.78
	43.92298

	1303.15
	-5.31137
	1303.61
	-55.6087
	1303.44
	33.99509
	1303.44
	39.54046
	1303.44
	47.92462
	1303.44
	62.90682
	1303.44
	-35.2126
	1303.44
	42.72354

	1303.81
	-5.25243
	1304.28
	-55.6776
	1304.11
	33.49369
	1304.11
	39.53666
	1304.11
	48.39561
	1304.11
	63.0297
	1304.11
	-34.5036
	1304.11
	42.36074

	1304.48
	-5.19249
	1304.95
	-55.2504
	1304.78
	33.61405
	1304.78
	39.63797
	1304.78
	49.61504
	1304.78
	63.25767
	1304.78
	-33.0462
	1304.78
	42.61971

	1305.15
	-5.13222
	1305.62
	-54.8501
	1305.45
	32.30753
	1305.45
	39.48548
	1305.45
	49.49136
	1305.45
	63.23184
	1305.45
	-32.9319
	1305.45
	41.4518

	1305.82
	-5.07185
	1306.28
	-54.2993
	1306.12
	34.14866
	1306.12
	38.56122
	1306.12
	47.9841
	1306.12
	62.43425
	1306.12
	-34.2012
	1306.12
	43.43154

	1306.48
	-5.01162
	1306.95
	-56.794
	1306.79
	34.77508
	1306.79
	38.53363
	1306.79
	45.91345
	1306.79
	62.53333
	1306.79
	-36.0338
	1306.79
	44.19657

	1307.15
	-4.95151
	1307.62
	-57.5834
	1307.45
	35.96081
	1307.45
	38.66981
	1307.45
	44.37345
	1307.45
	62.79429
	1307.45
	-37.3394
	1307.45
	45.51884

	1307.82
	-4.89156
	1308.29
	-56.9636
	1308.12
	37.21584
	1308.12
	37.38411
	1308.12
	45.91985
	1308.12
	61.63525
	1308.12
	-35.555
	1308.12
	46.91248

	1308.48
	-4.8321
	1308.95
	-57.6808
	1308.79
	37.67283
	1308.79
	38.63762
	1308.79
	46.5264
	1308.79
	63.01543
	1308.79
	-34.7104
	1308.79
	47.50809

	1309.15
	-4.77344
	1309.62
	-57.9166
	1309.46
	38.36314
	1309.46
	39.91792
	1309.46
	44.43141
	1309.46
	64.4224
	1309.46
	-36.5674
	1309.46
	48.337

	1309.82
	-4.71556
	1310.29
	-58.4186
	1310.13
	38.61953
	1310.13
	41.37057
	1310.13
	45.13323
	1310.13
	66.00171
	1310.13
	-35.6276
	1310.13
	48.732

	1310.48
	-4.65858
	1310.96
	-59.3356
	1310.79
	39.14092
	1310.79
	41.49903
	1310.79
	43.97601
	1310.79
	66.25495
	1310.79
	-36.5504
	1310.79
	49.38994

	1311.15
	-4.60264
	1311.63
	-59.3684
	1311.46
	40.80729
	1311.46
	39.92043
	1311.46
	42.3686
	1311.46
	64.80302
	1311.46
	-37.9198
	1311.46
	51.19492

	1311.81
	-4.54789
	1312.29
	-60.3447
	1312.13
	40.00895
	1312.13
	40.20654
	1312.13
	42.22408
	1312.13
	65.21579
	1312.13
	-37.8263
	1312.13
	50.53519

	1312.48
	-4.49431
	1312.96
	-61.0625
	1312.8
	39.71844
	1312.8
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	-0.17255
	1365.99
	-2.89962
	1365.99
	-12.1933
	1365.99
	11.48007
	1365.99
	-107.394
	1365.99
	16.89332

	1365.96
	-5.12421
	1366.78
	-68.3551
	1366.65
	0.34991
	1366.65
	-4.2659
	1366.65
	-14.9538
	1366.65
	9.47162
	1366.65
	-110.895
	1366.65
	17.39442

	1366.62
	-5.18647
	1367.44
	-67.8249
	1367.31
	-0.3196
	1367.31
	-3.88492
	1367.31
	-15.7107
	1367.31
	9.21043
	1367.31
	-112.392
	1367.31
	16.70356

	1367.28
	-5.24889
	1368.11
	-68.3099
	1367.97
	0.23719
	1367.97
	-3.1735
	1367.97
	-14.7042
	1367.97
	9.27968
	1367.97
	-112.125
	1367.97
	17.23899

	1367.94
	-5.31149
	1368.77
	-68.5969
	1368.63
	-0.07426
	1368.63
	-1.7111
	1368.63
	-12.9683
	1368.63
	10.09991
	1368.63
	-111.129
	1368.63
	16.90618

	1368.61
	-5.37403
	1369.43
	-68.3989
	1369.3
	-1.04971
	1369.3
	-1.94505
	1369.3
	-13.5034
	1369.3
	9.21406
	1369.3
	-112.415
	1369.3
	15.90906

	1369.27
	-5.43661
	1370.09
	-68.519
	1369.96
	-1.23879
	1369.96
	-2.1777
	1369.96
	-14.1313
	1369.96
	8.33924
	1369.96
	-113.783
	1369.96
	15.69862

	1369.93
	-5.49923
	1370.75
	-68.0642
	1370.62
	-1.72259
	1370.62
	-3.00702
	1370.62
	-14.8459
	1370.62
	6.86776
	1370.62
	-115.238
	1370.62
	15.19347

	1370.59
	-5.56188
	1371.41
	-69.1709
	1371.28
	-2.5456
	1371.28
	-4.543
	1371.28
	-16.2223
	1371.28
	4.68961
	1371.28
	-117.354
	1371.28
	14.3491

	1371.26
	-5.62453
	1372.07
	-69.4639
	1371.94
	-2.78702
	1371.94
	-3.5007
	1371.94
	-15.9258
	1371.94
	5.08974
	1371.94
	-117.798
	1371.94
	14.08632

	1371.92
	-5.68711
	1372.74
	-67.6209
	1372.6
	-2.77337
	1372.6
	-3.07825
	1372.6
	-16.2499
	1372.6
	4.87002
	1372.6
	-118.862
	1372.6
	14.07862

	1372.58
	-5.74966
	1373.4
	-67.3532
	1373.27
	-2.83701
	1373.27
	-2.64224
	1373.27
	-16.6988
	1373.27
	4.65413
	1373.27
	-120.062
	1373.27
	13.9933

	1373.24
	-5.81194
	1374.06
	-66.5138
	1373.93
	-2.82922
	1373.93
	-2.42131
	1373.93
	-19.1639
	1373.93
	4.23289
	1373.93
	-123.267
	1373.93
	13.97973

	1373.91
	-5.8742
	1374.72
	-66.5496
	1374.59
	-2.98691
	1374.59
	-1.38739
	1374.59
	-20.226
	1374.59
	4.62464
	1374.59
	-125.069
	1374.59
	13.80068

	1374.57
	-5.9365
	1375.38
	-68.1304
	1375.25
	-2.46911
	1375.25
	-0.08857
	1375.25
	-16.9969
	1375.25
	5.28129
	1375.25
	-122.58
	1375.25
	14.29713

	1375.23
	-5.9985
	1376.04
	-68.3555
	1375.91
	-0.77091
	1375.91
	0.22247
	1375.91
	-17.5707
	1375.91
	5.25271
	1375.91
	-123.894
	1375.91
	15.97397

	1375.89
	-6.05996
	1376.7
	-67.5761
	1376.57
	0.13063
	1376.57
	0.1509
	1376.57
	-16.76
	1376.57
	4.89255
	1376.57
	-123.823
	1376.57
	16.85415

	1376.55
	-6.12109
	1377.36
	-67.7856
	1377.23
	1.48255
	1377.23
	1.49326
	1377.23
	-16.2314
	1377.23
	5.94631
	1377.23
	-124.035
	1377.23
	18.18473

	1377.22
	-6.18187
	1378.02
	-67.62
	1377.9
	1.96639
	1377.9
	2.85905
	1377.9
	-16.913
	1377.9
	7.01914
	1377.9
	-125.467
	1377.9
	18.64688

	1377.88
	-6.24195
	1378.69
	-68.4204
	1378.56
	3.76244
	1378.56
	3.78499
	1378.56
	-15.3733
	1378.56
	7.65649
	1378.56
	-124.668
	1378.56
	20.42158

	1378.54
	-6.30141
	1379.35
	-68.9567
	1379.22
	6.06144
	1379.22
	4.07092
	1379.22
	-14.429
	1379.22
	7.65383
	1379.22
	-124.464
	1379.22
	22.69922

	1379.2
	-6.36026
	1380.01
	-69.4682
	1379.88
	7.08691
	1379.88
	5.68921
	1379.88
	-12.447
	1379.88
	8.98353
	1379.88
	-123.222
	1379.88
	23.70334

	1379.86
	-6.41835
	1380.67
	-69.2569
	1380.54
	6.79494
	1380.54
	6.09735
	1380.54
	-11.682
	1380.54
	9.10308
	1380.54
	-123.197
	1380.54
	23.39001

	1380.52
	-6.47577
	1381.33
	-68.0312
	1381.2
	7.89689
	1381.2
	7.52667
	1381.2
	-11.5602
	1381.2
	10.2438
	1381.2
	-123.815
	1381.2
	24.47061

	1381.18
	-6.53214
	1381.99
	-68.1663
	1381.86
	9.21826
	1381.86
	7.51579
	1381.86
	-11.1606
	1381.86
	9.94434
	1381.86
	-124.155
	1381.86
	25.77061

	1381.85
	-6.58753
	1382.65
	-67.8356
	1382.52
	9.65884
	1382.52
	8.7253
	1382.52
	-9.75976
	1382.52
	10.86526
	1382.52
	-123.494
	1382.52
	26.18984

	1382.51
	-6.64197
	1383.31
	-67.4095
	1383.18
	11.00766
	1383.18
	9.48565
	1383.18
	-8.56959
	1383.18
	11.33702
	1383.18
	-123.044
	1383.18
	27.51731

	1383.17
	-6.69548
	1383.97
	-66.8694
	1383.84
	12.97904
	1383.84
	10.08639
	1383.84
	-6.59098
	1383.84
	11.64916
	1383.84
	-121.805
	1383.84
	29.46732

	1383.83
	-6.7481
	1384.63
	-66.7866
	1384.5
	13.30729
	1384.5
	11.32973
	1384.5
	-6.00582
	1384.5
	12.60391
	1384.5
	-121.96
	1384.5
	29.77422

	1384.49
	-6.79929
	1385.29
	-65.1116
	1385.16
	14.32201
	1385.16
	12.33581
	1385.16
	-5.22615
	1385.16
	13.32141
	1385.16
	-121.921
	1385.16
	30.76758

	1385.15
	-6.84916
	1385.95
	-64.1606
	1385.82
	15.38398
	1385.82
	13.12013
	1385.82
	-4.84002
	1385.82
	13.81714
	1385.82
	-122.275
	1385.82
	31.8082

	1385.81
	-6.89759
	1386.61
	-63.8928
	1386.48
	14.60832
	1386.48
	13.16783
	1386.48
	-4.34615
	1386.48
	13.57625
	1386.48
	-122.521
	1386.48
	31.01119

	1386.47
	-6.94439
	1387.27
	-63.7043
	1387.14
	14.77148
	1387.14
	14.33632
	1387.14
	-3.03111
	1387.14
	14.45614
	1387.14
	-121.946
	1387.14
	31.15299

	1387.13
	-6.98958
	1387.93
	-63.9577
	1387.81
	15.87046
	1387.81
	15.68839
	1387.81
	-3.22055
	1387.81
	15.51526
	1387.81
	-122.886
	1387.81
	32.23029

	1387.8
	-7.03316
	1388.59
	-64.7751
	1388.46
	16.64565
	1388.46
	15.16055
	1388.46
	-3.50162
	1388.46
	14.70319
	1388.46
	-123.896
	1388.46
	32.98445

	1388.46
	-7.07515
	1389.25
	-64.3532
	1389.13
	18.04327
	1389.13
	16.77777
	1389.13
	-1.80176
	1389.13
	16.02745
	1389.13
	-122.947
	1389.13
	34.36039

	1389.12
	-7.11552
	1389.91
	-64.4936
	1389.78
	19.43769
	1389.78
	17.48605
	1389.78
	0.45489
	1389.78
	16.45152
	1389.78
	-121.42
	1389.78
	35.73377

	1389.78
	-7.15403
	1390.57
	-64.2339
	1390.45
	20.93532
	1390.45
	17.64294
	1390.45
	-0.28811
	1390.45
	16.31544
	1390.45
	-122.914
	1390.45
	37.20972

	1390.44
	-7.19074
	1391.23
	-64.5438
	1391.1
	23.17053
	1391.1
	17.0446
	1391.1
	0.13117
	1391.1
	15.43288
	1391.1
	-123.223
	1391.1
	39.42391

	1391.1
	-7.22556
	1391.89
	-63.7446
	1391.76
	23.89862
	1391.76
	17.1028
	1391.76
	-0.26579
	1391.76
	15.20249
	1391.76
	-124.36
	1391.76
	40.13064

	1391.76
	-7.25875
	1392.55
	-64.6674
	1392.42
	24.42103
	1392.42
	17.88001
	1392.42
	-0.28882
	1392.42
	15.69111
	1392.42
	-125.123
	1392.42
	40.63168

	1392.42
	-7.29039
	1393.2
	-64.4455
	1393.08
	23.54344
	1393.08
	18.54453
	1393.08
	-0.10836
	1393.08
	16.06704
	1393.08
	-125.408
	1393.08
	39.73274

	1393.08
	-7.32047
	1393.86
	-64.2467
	1393.74
	23.00899
	1393.74
	19.39199
	1393.74
	0.38663
	1393.74
	16.62591
	1393.74
	-124.902
	1393.74
	39.17694

	1393.74
	-7.34909
	1394.52
	-64.921
	1394.4
	24.08003
	1394.4
	21.52102
	1394.4
	-0.03604
	1394.4
	18.46635
	1394.4
	-125.313
	1394.4
	40.22662

	1394.4
	-7.3765
	1395.18
	-64.1638
	1395.06
	24.90305
	1395.06
	22.37422
	1395.06
	1.09725
	1395.06
	19.03096
	1395.06
	-124.168
	1395.06
	41.02828

	1395.06
	-7.4028
	1395.84
	-64.8917
	1395.72
	25.48352
	1395.72
	24.3406
	1395.72
	2.74808
	1395.72
	20.70875
	1395.72
	-122.505
	1395.72
	41.5874

	1395.72
	-7.42788
	1396.5
	-66.2496
	1396.38
	25.67714
	1396.38
	24.99424
	1396.38
	4.84695
	1396.38
	21.0738
	1396.38
	-120.395
	1396.38
	41.75966

	1396.38
	-7.45129
	1397.16
	-65.296
	1397.04
	26.10251
	1397.04
	25.93769
	1397.04
	4.97542
	1397.04
	21.72866
	1397.04
	-120.254
	1397.04
	42.16368

	1397.04
	-7.47289
	1397.82
	-64.6667
	1397.7
	26.95946
	1397.7
	26.85799
	1397.7
	5.01095
	1397.7
	22.36037
	1397.7
	-120.207
	1397.7
	42.99927

	1397.7
	-7.49265
	1398.48
	-64.0882
	1398.36
	26.9127
	1398.36
	26.56325
	1398.36
	4.55695
	1398.36
	21.77704
	1398.36
	-120.65
	1398.36
	42.93115

	1398.36
	-7.51048
	1399.14
	-65.1567
	1399.02
	28.26181
	1399.02
	28.80282
	1399.02
	5.16727
	1399.02
	23.72802
	1399.02
	-120.028
	1399.02
	44.25891

	1399.02
	-7.52621
	1399.79
	-64.1829
	1399.68
	29.39897
	1399.68
	29.81926
	1399.68
	6.47621
	1399.68
	24.45587
	1399.68
	-118.707
	1399.68
	45.37471

	1399.68
	-7.53977
	1400.45
	-63.2797
	1400.34
	30.69004
	1400.34
	31.99805
	1400.34
	8.39476
	1400.34
	26.34606
	1400.34
	-116.777
	1400.34
	46.64443

	1400.34
	-7.55129
	1401.11
	-64.5424
	1400.99
	33.06198
	1400.99
	31.70937
	1400.99
	7.44573
	1400.99
	25.77317
	1400.99
	-117.714
	1400.99
	48.99534

	1401
	-7.56067
	1401.77
	-64.4253
	1401.65
	33.08072
	1401.65
	31.92429
	1401.65
	8.77985
	1401.65
	25.6995
	1401.65
	-116.368
	1401.65
	48.99272

	1401.66
	-7.56795
	1402.43
	-64.308
	1402.31
	35.11789
	1402.31
	32.13587
	1402.31
	8.37966
	1402.31
	25.62249
	1402.31
	-116.757
	1402.31
	51.00853

	1402.32
	-7.57319
	1403.09
	-62.8208
	1402.97
	36.62937
	1402.97
	32.2955
	1402.97
	8.53005
	1402.97
	25.49352
	1402.97
	-116.595
	1402.97
	52.49865

	1402.97
	-7.57639
	1403.74
	-61.0983
	1403.63
	37.54851
	1403.63
	32.51674
	1403.63
	7.79641
	1403.63
	25.42617
	1403.63
	-117.317
	1403.63
	53.39644

	1403.63
	-7.57763
	1404.4
	-61.942
	1404.29
	38.31764
	1404.29
	33.94896
	1404.29
	7.44042
	1404.29
	26.56981
	1404.29
	-117.661
	1404.29
	54.14422

	1404.29
	-7.57684
	1405.06
	-62.5386
	1404.95
	38.16876
	1404.95
	36.29162
	1404.95
	7.77018
	1404.95
	28.62388
	1404.95
	-117.32
	1404.95
	53.97397

	1404.95
	-7.57422
	1405.72
	-63.2368
	1405.6
	39.06856
	1405.6
	37.41893
	1405.6
	8.02464
	1405.6
	29.46697
	1405.6
	-117.054
	1405.6
	54.85275

	1405.61
	-7.56988
	1406.38
	-61.5872
	1406.26
	40.86792
	1406.26
	38.08988
	1406.26
	7.27822
	1406.26
	29.84933
	1406.26
	-117.789
	1406.26
	56.63075

	1406.27
	-7.5638
	1407.03
	-62.0029
	1406.92
	41.40276
	1406.92
	39.16588
	1406.92
	7.43485
	1406.92
	30.63674
	1406.92
	-117.62
	1406.92
	57.14423

	1406.93
	-7.55593
	1407.69
	-63.8464
	1407.58
	41.68978
	1407.58
	39.22668
	1407.58
	7.32517
	1407.58
	30.40895
	1407.58
	-117.718
	1407.58
	57.40989

	1407.59
	-7.54584
	1408.35
	-63.3669
	1408.24
	41.67247
	1408.24
	40.96685
	1408.24
	8.49717
	1408.24
	31.86052
	1408.24
	-116.535
	1408.24
	57.37123

	1408.25
	-7.53378
	1409.01
	-63.1845
	1408.9
	42.24065
	1408.9
	41.36956
	1408.9
	7.04192
	1408.9
	31.97465
	1408.9
	-117.978
	1408.9
	57.91806

	1408.91
	-7.51993
	1409.67
	-62.9308
	1409.55
	42.09421
	1409.55
	42.11246
	1409.55
	6.96105
	1409.55
	32.43333
	1409.55
	-118.048
	1409.55
	57.75058

	1409.56
	-7.50432
	1410.32
	-64.1279
	1410.21
	42.91907
	1410.21
	42.69307
	1410.21
	6.8596
	1410.21
	32.72535
	1410.21
	-118.137
	1410.21
	58.55409

	1410.22
	-7.48817
	1410.98
	-65.5806
	1410.87
	43.5604
	1410.87
	42.37858
	1410.87
	6.686
	1410.87
	32.12227
	1410.87
	-118.299
	1410.87
	59.17406

	1410.88
	-7.47146
	1411.64
	-64.7333
	1411.53
	42.95213
	1411.53
	42.62433
	1411.53
	5.92699
	1411.53
	32.07943
	1411.53
	-119.047
	1411.53
	58.54444

	1411.54
	-7.45412
	1412.29
	-64.2599
	1412.18
	43.1008
	1412.18
	42.57571
	1412.18
	5.36129
	1412.18
	31.74659
	1412.18
	-119.601
	1412.18
	58.67207

	1412.2
	-7.43587
	1412.95
	-64.838
	1412.84
	42.38804
	1412.84
	44.32975
	1412.84
	4.71295
	1412.84
	33.21204
	1412.84
	-120.237
	1412.84
	57.93795

	1412.86
	-7.41675
	1413.61
	-66.6176
	1413.5
	41.87645
	1413.5
	45.04752
	1413.5
	5.27303
	1413.5
	33.64122
	1413.5
	-119.666
	1413.5
	57.40501

	1413.51
	-7.39693
	1414.27
	-67.8962
	1414.16
	43.43231
	1414.16
	45.83038
	1414.16
	4.07763
	1414.16
	34.13549
	1414.16
	-120.849
	1414.16
	58.93952

	1414.17
	-7.37632
	1414.92
	-67.6702
	1414.81
	44.00885
	1414.81
	46.7603
	1414.81
	5.73052
	1414.81
	34.78119
	1414.81
	-119.185
	1414.81
	59.49502

	1414.83
	-7.35473
	1415.58
	-67.4835
	1415.47
	44.10747
	1415.47
	48.64027
	1415.47
	6.18873
	1415.47
	36.37257
	1415.47
	-118.715
	1415.47
	59.57228

	1415.49
	-7.33175
	1416.24
	-67.6304
	1416.13
	44.09688
	1416.13
	50.36343
	1416.13
	6.49603
	1416.13
	37.80714
	1416.13
	-118.396
	1416.13
	59.54035

	1416.15
	-7.30744
	1416.9
	-68.1282
	1416.79
	43.89787
	1416.79
	51.54091
	1416.79
	6.47647
	1416.79
	38.69603
	1416.79
	-118.404
	1416.79
	59.31998

	1416.8
	-7.28178
	1417.55
	-67.5618
	1417.44
	42.16992
	1417.44
	52.44151
	1417.44
	6.50364
	1417.44
	39.31241
	1417.44
	-118.365
	1417.44
	57.57099

	1417.46
	-7.25448
	1418.21
	-67.4436
	1418.1
	41.90875
	1418.1
	52.99879
	1418.1
	6.79976
	1418.1
	39.5811
	1418.1
	-118.058
	1418.1
	57.28846

	1418.12
	-7.22553
	1418.87
	-68.1917
	1418.76
	41.61797
	1418.76
	55.10371
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	1523.72
	-2.19107
	1523.72
	-0.15377
	1523.72
	-76.7769
	1523.72
	-158.134
	1523.72
	-31.441

	1523.84
	2.56758
	1524.41
	-75.1763
	1524.36
	3.11279
	1524.36
	-2.5298
	1524.36
	0.30767
	1524.36
	-78.6297
	1524.36
	-159.308
	1524.36
	-32.9468

	1524.48
	2.61979
	1525.06
	-75.7448
	1525.01
	4.17632
	1525.01
	-2.38684
	1525.01
	-0.05246
	1525.01
	-80.0246
	1525.01
	-161.329
	1525.01
	-32.9472

	1525.13
	2.67218
	1525.71
	-75.6174
	1525.66
	4.07778
	1525.66
	-3.87603
	1525.66
	-0.2437
	1525.66
	-83.0515
	1525.66
	-163.181
	1525.66
	-34.1097

	1525.78
	2.72506
	1526.35
	-75.8058
	1526.3
	4.99327
	1526.3
	-4.21986
	1526.3
	0.21873
	1526.3
	-84.9095
	1526.3
	-164.354
	1526.3
	-34.2418

	1526.42
	2.77873
	1527
	-76.594
	1526.95
	5.2258
	1526.95
	-4.03925
	1526.95
	0.63365
	1526.95
	-86.2667
	1526.95
	-165.6
	1526.95
	-35.0733

	1527.07
	2.83305
	1527.64
	-77.1312
	1527.59
	4.08333
	1527.59
	-5.07602
	1527.59
	1.74948
	1527.59
	-88.8176
	1527.59
	-166.12
	1527.59
	-37.2633

	1527.72
	2.88781
	1528.29
	-77.2718
	1528.24
	3.62712
	1528.24
	-5.36972
	1528.24
	2.23173
	1528.24
	-90.649
	1528.24
	-167.298
	1528.24
	-38.7835

	1528.36
	2.94305
	1528.94
	-77.0376
	1528.89
	3.9271
	1528.89
	-5.87558
	1528.89
	4.12116
	1528.89
	-92.6927
	1528.89
	-167.07
	1528.89
	-39.5475

	1529.01
	2.9987
	1529.58
	-76.8607
	1529.53
	4.71668
	1529.53
	-7.21902
	1529.53
	4.39785
	1529.53
	-95.5502
	1529.53
	-168.428
	1529.53
	-39.8055

	1529.66
	3.05451
	1530.23
	-77.2023
	1530.18
	4.11094
	1530.18
	-6.89958
	1530.18
	5.44743
	1530.18
	-96.7686
	1530.18
	-169.04
	1530.18
	-41.4752

	1530.31
	3.11074
	1530.87
	-78.6296
	1530.83
	4.69285
	1530.83
	-7.69897
	1530.83
	5.33407
	1530.83
	-99.1058
	1530.83
	-170.814
	1530.83
	-41.9572

	1530.95
	3.16723
	1531.52
	-78.4399
	1531.47
	4.1033
	1531.47
	-8.4728
	1531.47
	5.32182
	1531.47
	-101.394
	1531.47
	-172.462
	1531.47
	-43.5944

	1531.6
	3.22368
	1532.16
	-79.4338
	1532.12
	3.45031
	1532.12
	-9.68905
	1532.12
	4.19532
	1532.12
	-104.148
	1532.12
	-175.249
	1532.12
	-45.3113

	1532.25
	3.27988
	1532.81
	-79.9688
	1532.76
	2.87927
	1532.76
	-9.10681
	1532.76
	1.83059
	1532.76
	-105.08
	1532.76
	-179.249
	1532.76
	-46.9299

	1532.89
	3.33594
	1533.46
	-80.6157
	1533.41
	1.92402
	1533.41
	-9.51384
	1533.41
	0.47573
	1533.41
	-107.024
	1533.41
	-182.265
	1533.41
	-48.9491

	1533.54
	3.39189
	1534.1
	-80.7819
	1534.06
	1.24287
	1534.06
	-9.86578
	1534.06
	1.7246
	1534.06
	-108.914
	1534.06
	-182.677
	1534.06
	-50.6942

	1534.18
	3.44829
	1534.75
	-80.725
	1534.7
	0.90968
	1534.7
	-9.35059
	1534.7
	1.9285
	1534.7
	-109.913
	1534.7
	-184.108
	1534.7
	-52.075

	1534.83
	3.50523
	1535.39
	-80.1297
	1535.35
	1.38902
	1535.35
	-9.11469
	1535.35
	2.06254
	1535.35
	-111.215
	1535.35
	-185.635
	1535.35
	-52.6596

	1535.48
	3.56298
	1536.04
	-81.3432
	1535.99
	2.1856
	1535.99
	-8.76381
	1535.99
	2.08503
	1535.99
	-112.378
	1535.99
	-187.248
	1535.99
	-52.9107

	1536.12
	3.6213
	1536.68
	-82.1788
	1536.64
	2.20827
	1536.64
	-8.98301
	1536.64
	2.20025
	1536.64
	-114.135
	1536.64
	-188.793
	1536.64
	-53.9519

	1536.77
	3.68006
	1537.33
	-82.2973
	1537.28
	1.35897
	1537.28
	-8.41743
	1537.28
	2.13704
	1537.28
	-115.084
	1537.28
	-190.492
	1537.28
	-55.8488

	1537.42
	3.73915
	1537.97
	-81.3557
	1537.93
	1.66867
	1537.93
	-7.70996
	1537.93
	1.54908
	1537.93
	-115.914
	1537.93
	-192.741
	1537.93
	-56.6031

	1538.06
	3.79856
	1538.62
	-81.4976
	1538.57
	1.40592
	1538.57
	-8.01104
	1538.57
	0.08517
	1538.57
	-117.729
	1538.57
	-195.84
	1538.57
	-57.9134

	1538.71
	3.8582
	1539.26
	-81.0169
	1539.22
	1.28739
	1539.22
	-8.19475
	1539.22
	-2.36653
	1539.22
	-119.451
	1539.22
	-199.953
	1539.22
	-59.0959

	1539.35
	3.91791
	1539.91
	-81.1116
	1539.87
	0.39199
	1539.87
	-8.71531
	1539.87
	-4.39626
	1539.87
	-121.509
	1539.87
	-203.643
	1539.87
	-61.0553

	1540
	3.97739
	1540.55
	-79.8321
	1540.51
	-0.71047
	1540.51
	-9.52307
	1540.51
	-4.96362
	1540.51
	-123.831
	1540.51
	-205.846
	1540.51
	-63.2053

	1540.65
	4.03667
	1541.2
	-79.6642
	1541.16
	-0.85657
	1541.16
	-9.88167
	1541.16
	-7.12093
	1541.16
	-125.727
	1541.16
	-209.664
	1541.16
	-64.4154

	1541.29
	4.09577
	1541.84
	-79.8408
	1541.8
	-1.64433
	1541.8
	-9.73982
	1541.8
	-7.71574
	1541.8
	-127.1
	1541.8
	-211.894
	1541.8
	-66.2507

	1541.94
	4.15503
	1542.49
	-79.4757
	1542.45
	-2.42701
	1542.45
	-9.58627
	1542.45
	-7.93003
	1542.45
	-128.484
	1542.45
	-213.769
	1542.45
	-68.0974

	1542.58
	4.2139
	1543.13
	-78.9192
	1543.09
	-3.20507
	1543.09
	-9.95598
	1543.09
	-8.01477
	1543.09
	-130.368
	1543.09
	-215.489
	1543.09
	-69.923

	1543.23
	4.27233
	1543.78
	-78.1095
	1543.74
	-4.11501
	1543.74
	-9.96596
	1543.74
	-7.59671
	1543.74
	-131.915
	1543.74
	-216.732
	1543.74
	-71.8969

	1543.87
	4.33006
	1544.42
	-77.5996
	1544.38
	-4.93209
	1544.38
	-9.01078
	1544.38
	-7.43988
	1544.38
	-132.474
	1544.38
	-218.211
	1544.38
	-73.7616

	1544.52
	4.38674
	1545.06
	-79.3714
	1545.03
	-6.35214
	1545.03
	-8.69899
	1545.03
	-7.34959
	1545.03
	-133.7
	1545.03
	-219.781
	1545.03
	-76.2456

	1545.16
	4.44199
	1545.71
	-79.3782
	1545.67
	-7.31542
	1545.67
	-9.25714
	1545.67
	-6.76876
	1545.67
	-135.773
	1545.67
	-220.836
	1545.67
	-78.2564

	1545.81
	4.49569
	1546.35
	-79.2907
	1546.31
	-7.43948
	1546.31
	-9.98705
	1546.31
	-6.88147
	1546.31
	-138.017
	1546.31
	-222.584
	1546.31
	-79.4281

	1546.46
	4.54769
	1547
	-79.8456
	1546.96
	-8.60081
	1546.96
	-9.21036
	1546.96
	-5.82129
	1546.96
	-138.778
	1546.96
	-223.185
	1546.96
	-81.6534

	1547.1
	4.59761
	1547.64
	-80.9049
	1547.6
	-9.18204
	1547.6
	-8.90635
	1547.6
	-5.73863
	1547.6
	-139.988
	1547.6
	-224.737
	1547.6
	-83.2822

	1547.75
	4.64584
	1548.29
	-81.3247
	1548.25
	-9.73886
	1548.25
	-8.53771
	1548.25
	-6.20081
	1548.25
	-141.157
	1548.25
	-226.86
	1548.25
	-84.903

	1548.39
	4.69231
	1548.93
	-81.2294
	1548.89
	-9.86374
	1548.89
	-8.57487
	1548.89
	-6.20768
	1548.89
	-142.708
	1548.89
	-228.502
	1548.89
	-86.0754

	1549.04
	4.73678
	1549.57
	-82.135
	1549.54
	-9.44597
	1549.54
	-8.49368
	1549.54
	-7.18684
	1549.54
	-144.165
	1549.54
	-231.142
	1549.54
	-86.7216

	1549.68
	4.77922
	1550.22
	-82.24
	1550.18
	-9.7579
	1550.18
	-8.15281
	1550.18
	-6.92881
	1550.18
	-145.338
	1550.18
	-232.52
	1550.18
	-88.0812

	1550.33
	4.81979
	1550.86
	-82.4861
	1550.83
	-10.1173
	1550.83
	-8.32573
	1550.83
	-8.12084
	1550.83
	-147.049
	1550.83
	-235.373
	1550.83
	-89.5045

	1550.97
	4.85817
	1551.5
	-82.913
	1551.47
	-8.82895
	1551.47
	-8.2227
	1551.47
	-8.36371
	1551.47
	-148.46
	1551.47
	-237.251
	1551.47
	-89.2637

	1551.62
	4.89382
	1552.15
	-82.1636
	1552.11
	-8.48404
	1552.11
	-7.99183
	1552.11
	-8.35965
	1552.11
	-149.743
	1552.11
	-238.882
	1552.11
	-89.9664

	1552.26
	4.92639
	1552.79
	-83.2326
	1552.76
	-7.67089
	1552.76
	-9.31259
	1552.76
	-7.5056
	1552.76
	-152.602
	1552.76
	-239.689
	1552.76
	-90.2172

	1552.9
	4.95545
	1553.44
	-81.966
	1553.4
	-7.70599
	1553.4
	-9.618
	1553.4
	-5.10604
	1553.4
	-154.421
	1553.4
	-238.925
	1553.4
	-91.2999

	1553.55
	4.98109
	1554.08
	-81.1856
	1554.04
	-8.23383
	1554.04
	-9.28771
	1554.04
	-2.2261
	1554.04
	-155.605
	1554.04
	-237.68
	1554.04
	-92.8754

	1554.19
	5.00316
	1554.72
	-81.2826
	1554.69
	-7.84149
	1554.69
	-8.35044
	1554.69
	0.17794
	1554.69
	-156.206
	1554.69
	-236.651
	1554.69
	-93.547

	1554.84
	5.02151
	1555.37
	-80.2299
	1555.33
	-6.89482
	1555.33
	-8.42074
	1555.33
	0.0637
	1555.33
	-157.79
	1555.33
	-236.77
	1555.33
	-93.6479

	1555.48
	5.03581
	1556.01
	-80.369
	1555.98
	-5.95288
	1555.98
	-7.65916
	1555.98
	-1.42257
	1555.98
	-158.566
	1555.98
	-238.26
	1555.98
	-93.7699

	1556.13
	5.04596
	1556.65
	-82.2759
	1556.62
	-4.51623
	1556.62
	-5.7526
	1556.62
	-0.90666
	1556.62
	-158.174
	1556.62
	-237.748
	1556.62
	-93.3808

	1556.77
	5.05196
	1557.3
	-82.9083
	1557.26
	-3.91587
	1557.26
	-4.59487
	1557.26
	-1.00605
	1557.26
	-158.53
	1557.26
	-237.852
	1557.26
	-93.8281

	1557.42
	5.05387
	1557.94
	-83.2616
	1557.91
	-4.11944
	1557.91
	-2.37563
	1557.91
	1.09626
	1557.91
	-157.849
	1557.91
	-235.754
	1557.91
	-95.0956

	1558.06
	5.05131
	1558.58
	-83.9171
	1558.55
	-3.72064
	1558.55
	-0.60574
	1558.55
	2.59471
	1558.55
	-157.593
	1558.55
	-234.259
	1558.55
	-95.7444

	1558.7
	5.04411
	1559.23
	-84.7349
	1559.19
	-3.53019
	1559.19
	-0.01981
	1559.19
	3.2803
	1559.19
	-158.493
	1559.19
	-233.578
	1559.19
	-96.6015

	1559.35
	5.03201
	1559.87
	-82.7881
	1559.84
	-2.75042
	1559.84
	-0.15403
	1559.84
	5.52026
	1559.84
	-158.012
	1559.84
	-231.342
	1559.84
	-96.8857

	1559.99
	5.01533
	1560.51
	-84.914
	1560.48
	0.20331
	1560.48
	0.36435
	1560.48
	5.00181
	1560.48
	-156.887
	1560.48
	-231.864
	1560.48
	-94.8408

	1560.64
	4.994
	1561.15
	-85.0996
	1561.12
	0.96386
	1561.12
	0.35588
	1561.12
	7.02884
	1561.12
	-156.289
	1561.12
	-229.841
	1561.12
	-93.8734

	1561.28
	4.96789
	1561.8
	-84.4826
	1561.77
	0.65851
	1561.77
	0.37342
	1561.77
	9.64993
	1561.77
	-155.656
	1561.77
	-227.224
	1561.77
	-93.9686

	1561.92
	4.93701
	1562.44
	-84.3605
	1562.41
	0.64984
	1562.41
	0.43024
	1562.41
	11.84167
	1562.41
	-154.992
	1562.41
	-225.037
	1562.41
	-93.7703

	1562.57
	4.90113
	1563.08
	-83.7211
	1563.05
	0.93353
	1563.05
	0.59705
	1563.05
	14.374
	1563.05
	-154.219
	1563.05
	-222.509
	1563.05
	-93.2797

	1563.21
	4.86016
	1563.72
	-83.6244
	1563.7
	1.31504
	1563.7
	0.58675
	1563.7
	17.38431
	1563.7
	-153.614
	1563.7
	-219.502
	1563.7
	-92.6881

	1563.85
	4.81424
	1564.37
	-83.3641
	1564.34
	2.70371
	1564.34
	0.82278
	1564.34
	19.43809
	1564.34
	-152.771
	1564.34
	-217.453
	1564.34
	-91.0925

	1564.5
	4.76311
	1565.01
	-84.2463
	1564.98
	3.8407
	1564.98
	2.1645
	1564.98
	22.43958
	1564.98
	-150.823
	1564.98
	-214.455
	1564.98
	-89.7486

	1565.14
	4.70647
	1565.65
	-84.2576
	1565.62
	4.56985
	1565.62
	2.43191
	1565.62
	26.83049
	1565.62
	-149.949
	1565.62
	-210.068
	1565.62
	-88.8125

	1565.78
	4.64382
	1566.29
	-82.8891
	1566.27
	6.33134
	1566.27
	3.06004
	1566.27
	30.97605
	1566.27
	-148.705
	1566.27
	-205.927
	1566.27
	-86.8409

	1566.43
	4.5752
	1566.94
	-82.5437
	1566.91
	8.129
	1566.91
	2.23234
	1566.91
	35.01056
	1566.91
	-148.927
	1566.91
	-201.897
	1566.91
	-84.8363

	1567.07
	4.50058
	1567.58
	-81.8426
	1567.55
	9.17538
	1567.55
	0.74446
	1567.55
	37.08142
	1567.55
	-149.808
	1567.55
	-199.83
	1567.55
	-83.583

	1567.71
	4.4204
	1568.22
	-82.3705
	1568.19
	10.5303
	1568.19
	0.74461
	1568.19
	39.94809
	1568.19
	-149.201
	1568.19
	-196.967
	1568.19
	-82.0212

	1568.36
	4.33462
	1568.86
	-81.871
	1568.84
	11.14041
	1568.84
	1.30685
	1568.84
	42.33875
	1568.84
	-148.023
	1568.84
	-194.581
	1568.84
	-81.2009

	1569
	4.2434
	1569.5
	-83.2496
	1569.48
	12.26483
	1569.48
	1.62014
	1569.48
	45.64451
	1569.48
	-147.104
	1569.48
	-191.279
	1569.48
	-79.8696

	1569.64
	4.14674
	1570.15
	-84.5371
	1570.12
	13.66846
	1570.12
	0.84107
	1570.12
	47.95145
	1570.12
	-147.276
	1570.12
	-188.976
	1570.12
	-78.2591

	1570.29
	4.04494
	1570.79
	-84.121
	1570.76
	14.09542
	1570.76
	1.42475
	1570.76
	52.168
	1570.76
	-146.086
	1570.76
	-184.764
	1570.76
	-77.6252

	1570.93
	3.93775
	1571.43
	-83.7054
	1571.41
	14.48179
	1571.41
	0.95955
	1571.41
	56.90096
	1571.41
	-145.936
	1571.41
	-180.035
	1571.41
	-77.0287

	1571.57
	3.82526
	1572.07
	-82.9914
	1572.05
	15.07256
	1572.05
	1.50774
	1572.05
	61.39641
	1572.05
	-144.781
	1572.05
	-175.543
	1572.05
	-76.231

	1572.21
	3.70767
	1572.71
	-82.3674
	1572.69
	16.39812
	1572.69
	3.3071
	1572.69
	66.0986
	1572.69
	-142.375
	1572.69
	-170.845
	1572.69
	-74.6985

	1572.86
	3.58491
	1573.36
	-83.1354
	1573.33
	18.05114
	1573.33
	3.46333
	1573.33
	70.95157
	1573.33
	-141.613
	1573.33
	-165.996
	1573.33
	-72.8386

	1573.5
	3.45728
	1574
	-83.383
	1573.97
	19.53317
	1573.97
	5.32015
	1573.97
	74.52709
	1573.97
	-139.149
	1573.97
	-162.425
	1573.97
	-71.1497

	1574.14
	3.32531
	1574.64
	-84.3691
	1574.62
	19.44579
	1574.62
	6.4018
	1574.62
	79.43373
	1574.62
	-137.452
	1574.62
	-157.522
	1574.62
	-71.0269

	1574.79
	3.18959
	1575.28
	-85.9102
	1575.26
	20.95712
	1575.26
	7.18705
	1575.26
	83.30419
	1575.26
	-136.06
	1575.26
	-153.656
	1575.26
	-69.3087

	1575.43
	3.05031
	1575.92
	-86.1538
	1575.9
	22.66179
	1575.9
	8.50132
	1575.9
	88.46127
	1575.9
	-134.14
	1575.9
	-148.503
	1575.9
	-67.3971

	1576.07
	2.90759
	1576.56
	-85.8991
	1576.54
	24.73282
	1576.54
	9.70774
	1576.54
	90.44504
	1576.54
	-132.327
	1576.54
	-146.523
	1576.54
	-65.1191

	1576.71
	2.76145
	1577.2
	-85.7856
	1577.18
	26.13286
	1577.18
	9.39867
	1577.18
	94.73838
	1577.18
	-132.029
	1577.18
	-142.234
	1577.18
	-63.5122

	1577.35
	2.61166
	1577.84
	-86.2518
	1577.82
	28.58016
	1577.82
	10.58216
	1577.82
	98.21755
	1577.82
	-130.24
	1577.82
	-138.759
	1577.82
	-60.858

	1578
	2.45817
	1578.49
	-86.2038
	1578.47
	30.99334
	1578.47
	10.89636
	1578.47
	101.0615
	1578.47
	-129.309
	1578.47
	-135.919
	1578.47
	-58.2347

	1578.64
	2.30081
	1579.13
	-87.1102
	1579.11
	32.09464
	1579.11
	12.85415
	1579.11
	105.8978
	1579.11
	-126.745
	1579.11
	-131.087
	1579.11
	-56.9264

	1579.28
	2.13978
	1579.77
	-86.9174
	1579.75
	34.24045
	1579.75
	13.93921
	1579.75
	110.0675
	1579.75
	-125.054
	1579.75
	-126.921
	1579.75
	-54.5737

	1579.92
	1.97527
	1580.41
	-85.5865
	1580.39
	36.27673
	1580.39
	15.18857
	1580.39
	116.6184
	1580.39
	-123.198
	1580.39
	-120.374
	1580.39
	-52.3305

	1580.56
	1.80747
	1581.05
	-86.0224
	1581.03
	39.08438
	1581.03
	16.10911
	1581.03
	122.8447
	1581.03
	-121.671
	1581.03
	-114.152
	1581.03
	-49.316

	1581.21
	1.63712
	1581.69
	-86.6397
	1581.67
	41.76456
	1581.67
	18.01259
	1581.67
	128.2467
	1581.67
	-119.161
	1581.67
	-108.754
	1581.67
	-46.4289

	1581.85
	1.46472
	1582.33
	-85.4576
	1582.31
	44.47807
	1582.31
	19.85843
	1582.31
	135.3844
	1582.31
	-116.709
	1582.31
	-101.621
	1582.31
	-43.5085

	1582.49
	1.29036
	1582.97
	-87.245
	1582.95
	47.63578
	1582.95
	21.36132
	1582.95
	140.5356
	1582.95
	-114.6
	1582.95
	-96.4735
	1582.95
	-40.1438

	1583.13
	1.11451
	1583.61
	-87.5996
	1583.59
	50.06505
	1583.59
	23.28853
	1583.59
	147.5544
	1583.59
	-112.066
	1583.59
	-89.4587
	1583.59
	-37.5077

	1583.77
	0.93763
	1584.25
	-88.6795
	1584.24
	50.67558
	1584.24
	25.02018
	1584.24
	152.4079
	1584.24
	-109.719
	1584.24
	-84.6093
	1584.24
	-36.687

	1584.41
	0.7601
	1584.89
	-89.1633
	1584.88
	52.07386
	1584.88
	26.83386
	1584.88
	156.6484
	1584.88
	-107.298
	1584.88
	-80.3729
	1584.88
	-35.0818

	1585.06
	0.5817
	1585.53
	-88.5016
	1585.52
	54.12887
	1585.52
	29.4942
	1585.52
	160.6242
	1585.52
	-104.032
	1585.52
	-76.4012
	1585.52
	-32.8199

	1585.7
	0.40246
	1586.17
	-86.0863
	1586.16
	55.50055
	1586.16
	32.50965
	1586.16
	164.6035
	1586.16
	-100.41
	1586.16
	-72.426
	1586.16
	-31.2413

	1586.34
	0.22245
	1586.82
	-87.4937
	1586.8
	57.39516
	1586.8
	35.5347
	1586.8
	168.549
	1586.8
	-96.7784
	1586.8
	-68.4845
	1586.8
	-29.1398

	1586.98
	0.042
	1587.46
	-89.5733
	1587.44
	57.38261
	1587.44
	36.02112
	1587.44
	172.4556
	1587.44
	-95.6856
	1587.44
	-64.582
	1587.44
	-28.9454

	1587.62
	-0.13884
	1588.1
	-89.6179
	1588.08
	58.16073
	1588.08
	39.59146
	1588.08
	175.6446
	1588.08
	-91.5089
	1588.08
	-61.397
	1588.08
	-27.9604

	1588.26
	-0.31992
	1588.74
	-88.5906
	1588.72
	60.98904
	1588.72
	40.56925
	1588.72
	180.5214
	1588.72
	-89.9247
	1588.72
	-56.5243
	1588.72
	-24.9252

	1588.9
	-0.50105
	1589.38
	-88.5152
	1589.36
	62.65205
	1589.36
	41.10489
	1589.36
	183.7427
	1589.36
	-88.7827
	1589.36
	-53.3071
	1589.36
	-23.0552

	1589.54
	-0.68237
	1590.02
	-87.2698
	1590
	64.60034
	1590
	42.94484
	1590
	188.431
	1590
	-86.3363
	1590
	-48.6229
	1590
	-20.9

	1590.19
	-0.86371
	1590.66
	-86.0141
	1590.64
	66.45373
	1590.64
	42.99499
	1590.64
	191.301
	1590.64
	-85.6798
	1590.64
	-45.757
	1590.64
	-18.8397

	1590.83
	-1.04464
	1591.3
	-85.2423
	1591.28
	67.84346
	1591.28
	45.60396
	1591.28
	193.1606
	1591.28
	-82.4644
	1591.28
	-43.9014
	1591.28
	-17.2431

	1591.47
	-1.22502
	1591.94
	-84.3436
	1591.92
	68.9128
	1591.92
	46.2319
	1591.92
	196.0376
	1591.92
	-81.2301
	1591.92
	-41.0284
	1591.92
	-15.9668

	1592.11
	-1.4048
	1592.58
	-85.1446
	1592.56
	70.46448
	1592.56
	46.01841
	1592.56
	198.7752
	1592.56
	-80.8372
	1592.56
	-38.2949
	1592.56
	-14.2082

	1592.75
	-1.58418
	1593.21
	-85.5548
	1593.2
	70.63999
	1593.2
	47.46607
	1593.2
	203.0812
	1593.2
	-78.7831
	1593.2
	-33.9931
	1593.2
	-13.8258

	1593.39
	-1.7632
	1593.85
	-84.591
	1593.84
	71.76236
	1593.84
	47.72798
	1593.84
	205.2282
	1593.84
	-77.9148
	1593.84
	-31.8501
	1593.84
	-12.4966

	1594.03
	-1.94171
	1594.49
	-84.4879
	1594.48
	72.5002
	1594.48
	48.29553
	1594.48
	207.8374
	1594.48
	-76.7408
	1594.48
	-29.245
	1594.48
	-11.5518

	1594.67
	-2.1193
	1595.13
	-84.715
	1595.12
	73.04578
	1595.12
	49.15597
	1595.12
	208.9956
	1595.12
	-75.274
	1595.12
	-28.0908
	1595.12
	-10.7993

	1595.31
	-2.29601
	1595.77
	-84.4104
	1595.76
	74.3384
	1595.76
	49.90479
	1595.76
	209.9266
	1595.76
	-73.9188
	1595.76
	-27.1639
	1595.76
	-9.29977

	1595.95
	-2.47212
	1596.41
	-83.7417
	1596.4
	74.55493
	1596.4
	50.38708
	1596.4
	210.8694
	1596.4
	-72.8301
	1596.4
	-26.2252
	1596.4
	-8.87633

	1596.59
	-2.64783
	1597.05
	-83.8563
	1597.04
	75.92589
	1597.04
	50.986
	1597.04
	213.6877
	1597.04
	-71.6248
	1597.04
	-23.411
	1597.04
	-7.29846

	1597.23
	-2.82307
	1597.69
	-84.5509
	1597.68
	76.89683
	1597.68
	51.36802
	1597.68
	215.7529
	1597.68
	-70.6364
	1597.68
	-21.3498
	1597.68
	-6.12061

	1597.87
	-2.99763
	1598.33
	-83.716
	1598.32
	76.80385
	1598.32
	50.43958
	1598.32
	216.5885
	1598.32
	-70.9584
	1598.32
	-20.5182
	1598.32
	-6.00668

	1598.51
	-3.1715
	1598.97
	-83.5509
	1598.96
	76.58399
	1598.96
	51.24208
	1598.96
	216.8782
	1598.96
	-69.5495
	1598.96
	-20.2326
	1598.96
	-6.01963

	1599.15
	-3.34489
	1599.61
	-83.7144
	1599.6
	77.07276
	1599.6
	51.66844
	1599.6
	215.9412
	1599.6
	-68.5167
	1599.6
	-21.1737
	1599.6
	-5.32395

	1599.79
	-3.51755
	1600.25
	-83.1452
	1600.24
	77.27947
	1600.24
	53.54555
	1600.24
	219.2572
	1600.24
	-66.0332
	1600.24
	-17.8618
	1600.24
	-4.91033

	1600.43
	-3.68981
	1600.89
	-82.3771
	1600.88
	76.31155
	1600.88
	53.04967
	1600.88
	219.5899
	1600.88
	-65.9227
	1600.88
	-17.5331
	1600.88
	-5.67134

	1601.07
	-3.86163
	1601.52
	-81.0178
	1601.52
	76.46304
	1601.52
	54.07884
	1601.52
	220.2952
	1601.52
	-64.2871
	1601.52
	-16.8319
	1601.52
	-5.31294

	1601.71
	-4.03321
	1602.16
	-80.2793
	1602.16
	76.39197
	1602.16
	54.1103
	1602.16
	220.3513
	1602.16
	-63.6493
	1602.16
	-16.7798
	1602.16
	-5.1771

	1602.35
	-4.20447
	1602.8
	-80.2008
	1602.8
	76.3606
	1602.8
	53.909
	1602.8
	221.7264
	1602.8
	-63.2442
	1602.8
	-15.4088
	1602.8
	-5.00155

	1602.99
	-4.37555
	1603.44
	-80.4208
	1603.43
	77.04482
	1603.43
	53.18966
	1603.43
	220.6991
	1603.43
	-63.3666
	1603.43
	-16.4402
	1603.43
	-4.11366

	1603.63
	-4.54644
	1604.08
	-81.6768
	1604.07
	76.48227
	1604.07
	54.23001
	1604.07
	217.1821
	1604.07
	-61.7199
	1604.07
	-19.9612
	1604.07
	-4.4693

	1604.27
	-4.71919
	1604.19
	-82.6838
	1604.71
	75.49343
	1604.71
	53.89168
	1604.71
	215.7516
	1604.71
	-61.4518
	1604.71
	-21.3958
	1604.71
	-5.25122

	1604.91
	-4.89368
	1604.83
	-82.4381
	1605.35
	75.79901
	1605.35
	53.29685
	1605.35
	215.6373
	1605.35
	-61.4402
	1605.35
	-21.5142
	1605.35
	-4.73873

	1605.55
	-5.06952
	1605.47
	-82.3158
	1605.99
	75.80106
	1605.99
	53.63608
	1605.99
	212.8843
	1605.99
	-60.4946
	1605.99
	-24.2713
	1605.99
	-4.52978

	1606.19
	-5.24685
	1606.11
	-82.1292
	1606.63
	75.4976
	1606.63
	52.18565
	1606.63
	212.342
	1606.63
	-61.3386
	1606.63
	-24.8176
	1606.63
	-4.62632

	1606.83
	-5.42548
	1606.75
	-81.9795
	1607.27
	76.16003
	1607.27
	50.58693
	1607.27
	209.4603
	1607.27
	-62.3309
	1607.27
	-27.7034
	1607.27
	-3.75699

	1607.47
	-5.60516
	1607.39
	-83.0956
	1607.91
	75.77451
	1607.91
	49.22544
	1607.91
	206.3803
	1607.91
	-63.086
	1607.91
	-30.7875
	1607.91
	-3.9356

	1608.11
	-5.78548
	1608.03
	-85.0822
	1608.55
	74.48251
	1608.55
	48.71018
	1608.55
	202.8252
	1608.55
	-62.9949
	1608.55
	-34.3466
	1608.55
	-5.02068

	1608.75
	-5.96641
	1608.67
	-85.4493
	1609.18
	73.99178
	1609.18
	48.33786
	1609.18
	202.7561
	1609.18
	-62.7703
	1609.18
	-34.4197
	1609.18
	-5.30773

	1609.39
	-6.14794
	1609.31
	-86.3356
	1609.82
	74.08126
	1609.82
	48.94192
	1609.82
	199.6196
	1609.82
	-61.5598
	1609.82
	-37.5603
	1609.82
	-5.01135

	1610.03
	-6.33031
	1609.95
	-85.9956
	1610.46
	74.5219
	1610.46
	48.49357
	1610.46
	197.737
	1610.46
	-61.4018
	1610.46
	-39.4469
	1610.46
	-4.3638

	1610.66
	-6.51399
	1610.59
	-85.0797
	1611.1
	74.5641
	1611.1
	49.89262
	1611.1
	195.8805
	1611.1
	-59.3963
	1611.1
	-41.3075
	1611.1
	-4.11469

	1611.3
	-6.69913
	1611.23
	-82.2209
	1611.74
	73.64189
	1611.74
	48.67675
	1611.74
	192.7557
	1611.74
	-60.0058
	1611.74
	-44.4364
	1611.74
	-4.82998

	1611.94
	-6.88605
	1611.87
	-83.4962
	1612.38
	72.49753
	1612.38
	46.95944
	1612.38
	187.2858
	1612.38
	-61.1167
	1612.38
	-49.9103
	1612.38
	-5.76743

	1612.58
	-7.07507
	1612.51
	-84.0245
	1613.01
	70.62444
	1613.01
	44.82195
	1613.01
	182.9306
	1613.01
	-62.6573
	1613.01
	-54.2696
	1613.01
	-7.43685

	1613.22
	-7.26633
	1613.15
	-84.5296
	1613.65
	68.89274
	1613.65
	43.20888
	1613.65
	179.7497
	1613.65
	-63.664
	1613.65
	-57.4546
	1613.65
	-8.96164

	1613.86
	-7.45974
	1613.79
	-85.0917
	1614.29
	67.07123
	1614.29
	40.35223
	1614.29
	178.1317
	1614.29
	-65.9142
	1614.29
	-59.0766
	1614.29
	-10.5762

	1614.5
	-7.65524
	1614.43
	-84.543
	1614.93
	64.67913
	1614.93
	38.59395
	1614.93
	174.5277
	1614.93
	-67.0661
	1614.93
	-62.6847
	1614.93
	-12.7614

	1615.14
	-7.85274
	1615.07
	-82.8987
	1615.57
	61.79224
	1615.57
	38.08232
	1615.57
	170.305
	1615.57
	-66.9713
	1615.57
	-66.9115
	1615.57
	-15.4414

	1615.78
	-8.05241
	1615.71
	-84.1321
	1616.2
	59.98035
	1616.2
	36.4803
	1616.2
	165.2636
	1616.2
	-67.9764
	1616.2
	-71.9569
	1616.2
	-17.0496

	1616.41
	-8.25428
	1616.35
	-82.3496
	1616.84
	57.82533
	1616.84
	35.37407
	1616.84
	162.0638
	1616.84
	-68.4763
	1616.84
	-75.1608
	1616.84
	-18.9977

	1617.05
	-8.45826
	1616.99
	-83.202
	1617.48
	56.33777
	1617.48
	33.6674
	1617.48
	158.6081
	1617.48
	-69.5765
	1617.48
	-78.6205
	1617.48
	-20.2784

	1617.69
	-8.66428
	1617.62
	-83.6659
	1618.12
	53.23667
	1618.12
	32.77381
	1618.12
	154.8604
	1618.12
	-69.8637
	1618.12
	-82.3722
	1618.12
	-23.1726

	1618.33
	-8.87266
	1618.26
	-86.1213
	1618.75
	50.70422
	1618.75
	29.68359
	1618.75
	149.5425
	1618.75
	-72.357
	1618.75
	-87.6942
	1618.75
	-25.5013

	1618.97
	-9.08339
	1618.9
	-86.4151
	1619.39
	49.82794
	1619.39
	26.89482
	1619.39
	145.7242
	1619.39
	-74.5394
	1619.39
	-91.5166
	1619.39
	-26.1707

	1619.6
	-9.29645
	1619.54
	-86.2055
	1620.03
	49.13233
	1620.03
	26.73854
	1620.03
	141.0402
	1620.03
	-74.0893
	1620.03
	-96.2045
	1620.03
	-26.6594

	1620.24
	-9.51176
	1620.18
	-86.2164
	1620.67
	47.80233
	1620.67
	23.48577
	1620.67
	136.5051
	1620.67
	-76.7357
	1620.67
	-100.744
	1620.67
	-27.7825

	1620.88
	-9.72931
	1620.82
	-87.4671
	1621.3
	43.96261
	1621.3
	22.71928
	1621.3
	132.7832
	1621.3
	-76.9052
	1621.3
	-104.47
	1621.3
	-31.4185

	1621.52
	-9.94922
	1621.46
	-88.1936
	1621.94
	41.59586
	1621.94
	22.45075
	1621.94
	128.2545
	1621.94
	-76.5674
	1621.94
	-109.002
	1621.94
	-33.5784

	1622.16
	-10.1717
	1622.1
	-89.623
	1622.58
	39.62047
	1622.58
	21.27765
	1622.58
	123.3407
	1622.58
	-77.1341
	1622.58
	-113.92
	1622.58
	-35.3469

	1622.79
	-10.397
	1622.74
	-89.964
	1623.22
	37.82206
	1623.22
	20.77099
	1623.22
	119.0743
	1623.22
	-77.0343
	1623.22
	-118.191
	1623.22
	-36.9384

	1623.43
	-10.6254
	1623.38
	-91.665
	1623.85
	37.94491
	1623.85
	16.92022
	1623.85
	117.0519
	1623.85
	-80.2882
	1623.85
	-120.217
	1623.85
	-36.6118

	1624.07
	-10.8566
	1624.01
	-91.6619
	1624.49
	37.4867
	1624.49
	16.47763
	1624.49
	112.5546
	1624.49
	-80.1244
	1624.49
	-124.719
	1624.49
	-36.8631

	1624.71
	-11.0907
	1624.65
	-91.3744
	1625.13
	36.858
	1625.13
	14.74055
	1625.13
	105.8607
	1625.13
	-81.255
	1625.13
	-131.417
	1625.13
	-37.2849

	1625.35
	-11.3273
	1625.29
	-91.7196
	1625.76
	35.24399
	1625.76
	11.78841
	1625.76
	100.2009
	1625.76
	-83.6103
	1625.76
	-137.08
	1625.76
	-38.6953

	1625.98
	-11.5666
	1625.93
	-91.8746
	1626.4
	34.3451
	1626.4
	10.54016
	1626.4
	95.37618
	1626.4
	-84.2521
	1626.4
	-141.909
	1626.4
	-39.3872

	1626.62
	-11.809
	1626.57
	-93.0979
	1627.04
	34.33091
	1627.04
	9.32015
	1627.04
	88.79915
	1627.04
	-84.8657
	1627.04
	-148.49
	1627.04
	-39.1945

	1627.26
	-12.0545
	1627.21
	-92.4236
	1627.67
	32.84536
	1627.67
	8.14944
	1627.67
	83.93319
	1627.67
	-85.4395
	1627.67
	-153.36
	1627.67
	-40.4764

	1627.89
	-12.3029
	1627.84
	-93.1133
	1628.31
	30.66815
	1628.31
	5.48062
	1628.31
	77.64886
	1628.31
	-87.5019
	1628.31
	-159.649
	1628.31
	-42.4467

	1628.53
	-12.5544
	1628.48
	-93.7516
	1628.95
	30.34771
	1628.95
	2.54066
	1628.95
	72.37135
	1628.95
	-89.8355
	1628.95
	-164.93
	1628.95
	-42.5602

	1629.17
	-12.809
	1629.12
	-92.9985
	1629.58
	27.37451
	1629.58
	0.01074
	1629.58
	67.09284
	1629.58
	-91.7685
	1629.58
	-170.213
	1629.58
	-45.3297

	1629.81
	-13.0669
	1629.76
	-91.6393
	1630.22
	25.02936
	1630.22
	-2.17589
	1630.22
	63.22788
	1630.22
	-93.3487
	1630.22
	-174.082
	1630.22
	-47.468

	1630.44
	-13.3278
	1630.4
	-91.8664
	1630.86
	24.80755
	1630.86
	-2.59879
	1630.86
	58.34881
	1630.86
	-93.1652
	1630.86
	-178.965
	1630.86
	-47.4829

	1631.08
	-13.5915
	1631.04
	-91.538
	1631.49
	23.67751
	1631.49
	-5.08866
	1631.49
	53.51139
	1631.49
	-95.0582
	1631.49
	-183.806
	1631.49
	-48.4092

	1631.72
	-13.8572
	1631.67
	-90.4809
	1632.13
	21.86503
	1632.13
	-6.05761
	1632.13
	49.81777
	1632.13
	-95.4207
	1632.13
	-187.504
	1632.13
	-50.0148

	1632.35
	-14.1246
	1632.31
	-90.8122
	1632.76
	20.12636
	1632.76
	-7.94238
	1632.76
	45.53663
	1632.76
	-96.7086
	1632.76
	-191.789
	1632.76
	-51.5498

	1632.99
	-14.3936
	1632.95
	-90.6282
	1633.4
	19.82829
	1633.4
	-8.21405
	1633.4
	40.85394
	1633.4
	-96.3738
	1633.4
	-196.476
	1633.4
	-51.641

	1633.63
	-14.6638
	1633.59
	-90.0876
	1634.04
	18.77199
	1634.04
	-10.8806
	1634.04
	34.46949
	1634.04
	-98.434
	1634.04
	-202.864
	1634.04
	-52.4903

	1634.26
	-14.9352
	1634.22
	-90.2059
	1634.67
	18.04198
	1634.67
	-11.0485
	1634.67
	29.31239
	1634.67
	-98.005
	1634.67
	-208.025
	1634.67
	-53.0167

	1634.9
	-15.2074
	1634.86
	-90.2916
	1635.31
	17.66607
	1635.31
	-11.3668
	1635.31
	23.11911
	1635.31
	-97.7169
	1635.31
	-214.223
	1635.31
	-53.1857

	1635.54
	-15.48
	1635.5
	-90.6054
	1635.95
	16.34164
	1635.95
	-12.2481
	1635.95
	18.79325
	1635.95
	-97.9917
	1635.95
	-218.553
	1635.95
	-54.3032

	1636.17
	-15.7528
	1636.14
	-89.9566
	1636.58
	16.18241
	1636.58
	-14.6004
	1636.58
	15.39281
	1636.58
	-99.7472
	1636.58
	-221.957
	1636.58
	-54.2588

	1636.81
	-16.0258
	1636.77
	-90.4254
	1637.22
	15.48653
	1637.22
	-17.2942
	1637.22
	12.24396
	1637.22
	-101.835
	1637.22
	-225.11
	1637.22
	-54.7477

	1637.45
	-16.2988
	1637.41
	-90.1066
	1637.85
	13.58485
	1637.85
	-19.132
	1637.85
	9.14133
	1637.85
	-103.075
	1637.85
	-228.217
	1637.85
	-56.4457

	1638.08
	-16.5713
	1638.05
	-91.3366
	1638.49
	12.40269
	1638.49
	-18.926
	1638.49
	6.48915
	1638.49
	-102.263
	1638.49
	-230.873
	1638.49
	-57.421

	1638.72
	-16.8431
	1638.68
	-91.3307
	1639.12
	10.85603
	1639.12
	-19.7063
	1639.12
	2.19373
	1639.12
	-102.446
	1639.12
	-235.172
	1639.12
	-58.764

	1639.36
	-17.114
	1639.32
	-90.1056
	1639.76
	10.50026
	1639.76
	-18.4877
	1639.76
	-1.23281
	1639.76
	-100.621
	1639.76
	-238.603
	1639.76
	-58.9128

	1639.99
	-17.3838
	1639.96
	-90.3143
	1640.4
	10.44918
	1640.4
	-18.2168
	1640.4
	-1.9413
	1640.4
	-99.7441
	1640.4
	-239.316
	1640.4
	-58.757

	1640.63
	-17.6521
	1640.6
	-88.6479
	1641.03
	10.04263
	1641.03
	-19.6881
	1641.03
	-3.32068
	1641.03
	-100.618
	1641.03
	-240.699
	1641.03
	-58.9599

	1641.26
	-17.9185
	1641.23
	-88.334
	1641.67
	9.68128
	1641.67
	-19.1882
	1641.67
	-4.8402
	1641.67
	-99.5122
	1641.67
	-242.223
	1641.67
	-59.1143

	1641.9
	-18.183
	1641.87
	-88.3503
	1642.3
	9.28924
	1642.3
	-19.9178
	1642.3
	-4.5188
	1642.3
	-99.6448
	1642.3
	-241.905
	1642.3
	-59.3027

	1642.54
	-18.4451
	1642.51
	-87.6236
	1642.94
	8.62082
	1642.94
	-21.2419
	1642.94
	-6.45812
	1642.94
	-100.363
	1642.94
	-243.849
	1642.94
	-59.7642

	1643.17
	-18.7046
	1643.14
	-89.5588
	1643.57
	7.49536
	1643.57
	-23.0457
	1643.57
	-7.57676
	1643.57
	-101.569
	1643.57
	-244.971
	1643.57
	-60.686

	1643.81
	-18.9618
	1643.78
	-90.3444
	1644.21
	6.57216
	1644.21
	-22.7827
	1644.21
	-7.73769
	1644.21
	-100.7
	1644.21
	-245.136
	1644.21
	-61.4023

	1644.44
	-19.2164
	1644.42
	-90.113
	1644.84
	6.10061
	1644.84
	-22.7326
	1644.84
	-5.64829
	1644.84
	-100.053
	1644.84
	-243.051
	1644.84
	-61.6701

	1645.08
	-19.4685
	1645.05
	-90.6621
	1645.48
	5.19222
	1645.48
	-22.3216
	1645.48
	-6.54122
	1645.48
	-99.0356
	1645.48
	-243.948
	1645.48
	-62.3716

	1645.71
	-19.7181
	1645.69
	-92.8397
	1646.11
	4.61667
	1646.11
	-22.5291
	1646.11
	-8.81559
	1646.11
	-98.6462
	1646.11
	-246.226
	1646.11
	-62.7435

	1646.35
	-19.9655
	1646.33
	-92.9709
	1646.75
	5.05573
	1646.75
	-22.5588
	1646.75
	-10.8883
	1646.75
	-98.0695
	1646.75
	-248.303
	1646.75
	-62.0975

	1646.99
	-20.2107
	1646.96
	-91.6008
	1647.38
	5.08088
	1647.38
	-21.9057
	1647.38
	-12.6298
	1647.38
	-96.8195
	1647.38
	-250.048
	1647.38
	-61.8687

	1647.62
	-20.4533
	1647.6
	-92.5329
	1648.02
	4.72927
	1648.02
	-22.6425
	1648.02
	-12.9651
	1648.02
	-96.9499
	1648.02
	-250.388
	1648.02
	-62.0134

	1648.26
	-20.6933
	1648.24
	-93.1721
	1648.65
	4.7403
	1648.65
	-22.3102
	1648.65
	-14.584
	1648.65
	-96.0206
	1648.65
	-252.011
	1648.65
	-61.7987

	1648.89
	-20.9304
	1648.87
	-93.9997
	1649.28
	5.00427
	1649.28
	-22.7949
	1649.28
	-16.4422
	1649.28
	-95.9084
	1649.28
	-253.873
	1649.28
	-61.331

	1649.53
	-21.1642
	1649.51
	-94.1761
	1649.92
	3.97668
	1649.92
	-23.3689
	1649.92
	-16.844
	1649.92
	-95.876
	1649.92
	-254.279
	1649.92
	-62.1517

	1650.16
	-21.3942
	1650.14
	-93.1439
	1650.55
	5.25841
	1650.55
	-23.8377
	1650.55
	-17.674
	1650.55
	-95.748
	1650.55
	-255.113
	1650.55
	-60.6663

	1650.8
	-21.6205
	1650.78
	-93.4125
	1651.19
	6.25985
	1651.19
	-23.2896
	1651.19
	-17.3285
	1651.19
	-94.5934
	1651.19
	-254.771
	1651.19
	-59.4579

	1651.43
	-21.843
	1651.42
	-92.8204
	1651.82
	5.72345
	1651.82
	-22.6015
	1651.82
	-19.2022
	1651.82
	-93.3084
	1651.82
	-256.649
	1651.82
	-59.7907

	1652.07
	-22.0614
	1652.05
	-91.4335
	1652.46
	5.74157
	1652.46
	-23.3547
	1652.46
	-20.2444
	1652.46
	-93.4552
	1652.46
	-257.695
	1652.46
	-59.5656

	1652.7
	-22.2757
	1652.69
	-88.7832
	1653.09
	5.63929
	1653.09
	-22.917
	1653.09
	-20.8039
	1653.09
	-92.4206
	1653.09
	-258.259
	1653.09
	-59.4642

	1653.34
	-22.4853
	1653.32
	-88.195
	1653.72
	6.28143
	1653.72
	-22.7622
	1653.72
	-21.0357
	1653.72
	-91.6689
	1653.72
	-258.495
	1653.72
	-58.6184

	1653.97
	-22.69
	1653.96
	-88.0295
	1654.36
	6.18662
	1654.36
	-22.4627
	1654.36
	-19.7271
	1654.36
	-90.7629
	1654.36
	-257.19
	1654.36
	-58.5063

	1654.61
	-22.8897
	1654.59
	-87.7208
	1654.99
	6.93514
	1654.99
	-22.1524
	1654.99
	-19.0514
	1654.99
	-89.8557
	1654.99
	-256.518
	1654.99
	-57.5541

	1655.24
	-23.0846
	1655.23
	-88.3524
	1655.63
	7.41601
	1655.63
	-22.6089
	1655.63
	-19.5534
	1655.63
	-89.7058
	1655.63
	-257.024
	1655.63
	-56.8663

	1655.88
	-23.2746
	1655.87
	-88.5781
	1656.26
	6.34591
	1656.26
	-20.6076
	1656.26
	-20.0883
	1656.26
	-87.1076
	1656.26
	-257.563
	1656.26
	-57.7328

	1656.51
	-23.4601
	1656.5
	-88.4257
	1656.89
	5.73964
	1656.89
	-20.1089
	1656.89
	-21.0812
	1656.89
	-86.012
	1656.89
	-258.56
	1656.89
	-58.1354

	1657.15
	-23.6412
	1657.14
	-89.5927
	1657.53
	4.48641
	1657.53
	-20.0183
	1657.53
	-21.0571
	1657.53
	-85.3149
	1657.53
	-258.54
	1657.53
	-59.1817

	1657.78
	-23.8179
	1657.77
	-89.0998
	1658.16
	4.0374
	1658.16
	-19.1401
	1658.16
	-21.4825
	1658.16
	-83.8399
	1658.16
	-258.97
	1658.16
	-59.427

	1658.41
	-23.99
	1658.41
	-88.9788
	1658.8
	3.21065
	1658.8
	-17.9675
	1658.8
	-21.6921
	1658.8
	-82.0609
	1658.8
	-259.183
	1658.8
	-60.0468

	1659.05
	-24.1576
	1659.04
	-89.7694
	1659.43
	2.50449
	1659.43
	-17.2186
	1659.43
	-21.5491
	1659.43
	-80.715
	1659.43
	-259.044
	1659.43
	-60.5493

	1659.68
	-24.3208
	1659.68
	-91.6241
	1660.06
	2.90303
	1660.06
	-17.4041
	1660.06
	-20.0693
	1660.06
	-80.3036
	1660.06
	-257.569
	1660.06
	-59.9471

	1660.32
	-24.4795
	1660.31
	-93.2885
	1660.7
	3.91728
	1660.7
	-16.2074
	1660.7
	-19.1539
	1660.7
	-78.5005
	1660.7
	-256.657
	1660.7
	-58.7259

	1660.95
	-24.6338
	1660.95
	-94.4473
	1661.33
	4.12857
	1661.33
	-13.7717
	1661.33
	-19.1448
	1661.33
	-75.4679
	1661.33
	-256.652
	1661.33
	-58.311

	1661.59
	-24.784
	1661.58
	-95.747
	1661.96
	4.34135
	1661.96
	-12.1567
	1661.96
	-18.9874
	1661.96
	-73.256
	1661.96
	-256.499
	1661.96
	-57.8945

	1662.22
	-24.9301
	1662.22
	-95.6106
	1662.6
	5.51187
	1662.6
	-11.4756
	1662.6
	-20.1973
	1662.6
	-71.9685
	1662.6
	-257.713
	1662.6
	-56.5171

	1662.85
	-25.0722
	1662.85
	-93.308
	1663.23
	5.99828
	1663.23
	-11.1399
	1663.23
	-18.6326
	1663.23
	-71.0359
	1663.23
	-256.152
	1663.23
	-55.827

	1663.49
	-25.2102
	1663.49
	-92.8655
	1663.86
	5.94901
	1663.86
	-10.315
	1663.86
	-18.1293
	1663.86
	-69.6141
	1663.86
	-255.653
	1663.86
	-55.6726

	1664.12
	-25.3438
	1664.12
	-92.7019
	1664.5
	4.7914
	1664.5
	-10.332
	1664.5
	-18.0203
	1664.5
	-69.0246
	1664.5
	-255.548
	1664.5
	-56.6233

	1664.75
	-25.4725
	1664.76
	-92.8343
	1665.13
	4.2784
	1665.13
	-10.4033
	1665.13
	-19.9358
	1665.13
	-68.4991
	1665.13
	-257.467
	1665.13
	-56.9326

	1665.39
	-25.596
	1665.39
	-93.6561
	1665.76
	3.51227
	1665.76
	-10.6308
	1665.76
	-18.5209
	1665.76
	-68.1296
	1665.76
	-256.056
	1665.76
	-57.4951

	1666.02
	-25.7146
	1666.03
	-93.4856
	1666.4
	1.97889
	1666.4
	-9.64672
	1666.4
	-15.9594
	1666.4
	-66.5391
	1666.4
	-253.499
	1666.4
	-58.8215

	1666.66
	-25.8285
	1666.66
	-93.2287
	1667.03
	0.56659
	1667.03
	-9.36023
	1667.03
	-15.7845
	1667.03
	-65.6557
	1667.03
	-253.328
	1667.03
	-60.0302

	1667.29
	-25.9372
	1667.3
	-92.3205
	1667.66
	-0.10502
	1667.66
	-8.68861
	1667.66
	-12.9978
	1667.66
	-64.3872
	1667.66
	-250.545
	1667.66
	-60.4981

	1667.92
	-26.0408
	1667.93
	-91.1936
	1668.29
	0.02397
	1668.29
	-7.87601
	1668.29
	-11.4391
	1668.29
	-62.9776
	1668.29
	-248.991
	1668.29
	-60.1654

	1668.56
	-26.139
	1668.56
	-90.7705
	1668.93
	-0.6386
	1668.93
	-6.79188
	1668.93
	-9.26268
	1668.93
	-61.2871
	1668.93
	-246.818
	1668.93
	-60.6211

	1669.19
	-26.2318
	1669.2
	-92.7038
	1669.56
	0.14646
	1669.56
	-5.24968
	1669.56
	-6.10436
	1669.56
	-59.148
	1669.56
	-243.664
	1669.56
	-59.6324

	1669.82
	-26.3189
	1669.83
	-93.0969
	1670.19
	0.27407
	1670.19
	-3.98845
	1670.19
	-4.78879
	1670.19
	-57.2898
	1670.19
	-242.352
	1670.19
	-59.3011

	1670.46
	-26.4001
	1670.47
	-92.5984
	1670.82
	0.03297
	1670.82
	-3.88524
	1670.82
	-3.74482
	1670.82
	-56.5897
	1670.82
	-241.313
	1670.82
	-59.3385

	1671.09
	-26.4751
	1671.1
	-91.9001
	1671.46
	0.94902
	1671.46
	-3.67581
	1671.46
	-1.87981
	1671.46
	-55.7739
	1671.46
	-239.452
	1671.46
	-58.2155

	1671.72
	-26.544
	1671.73
	-90.0662
	1672.09
	1.61156
	1672.09
	-4.8012
	1672.09
	0.2296
	1672.09
	-56.3023
	1672.09
	-237.346
	1672.09
	-57.3493

	1672.36
	-26.6067
	1672.37
	-89.6999
	1672.72
	1.59429
	1672.72
	-4.71051
	1672.72
	0.12333
	1672.72
	-55.6147
	1672.72
	-237.456
	1672.72
	-57.1629

	1672.99
	-26.6635
	1673
	-89.9362
	1673.35
	1.93349
	1673.35
	-3.77903
	1673.35
	0
	1673.35
	-54.0863
	1673.35
	-237.584
	1673.35
	-56.62

	1673.62
	-26.714
	1673.64
	-89.6048
	1673.99
	1.46408
	1673.99
	-3.58406
	1673.99
	-2.13187
	1673.99
	-53.285
	1673.99
	-238.298
	1673.99
	-56.8825

	1674.25
	-26.7585
	1674.27
	-89.718
	1674.62
	-0.10485
	1674.62
	-3.53706
	1674.62
	-5.99179
	1674.62
	-52.641
	1674.62
	-240.762
	1674.62
	-58.2478

	1674.89
	-26.7972
	1674.9
	-90.4982
	1675.25
	-1.85994
	1675.25
	-1.92494
	1675.25
	-8.81665
	1675.25
	-50.432
	1675.25
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	-1.25282
	1675.88
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	-39.4983
	1685.99
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	-259.052
	1689.77
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	1690.4
	-255.172
	1690.4
	-60.7667

	1690.69
	-26.2019
	1690.73
	-88.4783
	1691.03
	-8.56241
	1691.03
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	24.22556
	1724.7
	-129.197
	1724.7
	5.58791

	1725.31
	-15.4227
	1725.4
	-88.0536
	1725.33
	45.63304
	1725.33
	56.81688
	1725.33
	-7.46369
	1725.33
	24.52222
	1725.33
	-129.893
	1725.33
	5.7057

	1725.94
	-15.1913
	1726.03
	-89.3359
	1725.96
	45.1294
	1725.96
	56.9293
	1725.96
	-6.09853
	1725.96
	24.80056
	1725.96
	-127.132
	1725.96
	5.4302

	1726.57
	-14.9624
	1726.66
	-90.018
	1726.59
	44.95184
	1726.59
	57.57329
	1726.59
	-6.50047
	1726.59
	25.61045
	1726.59
	-126.138
	1726.59
	5.48076

	1727.2
	-14.7357
	1727.29
	-91.1834
	1727.22
	45.2206
	1727.22
	57.37776
	1727.22
	-5.13751
	1727.22
	25.58083
	1727.22
	-123.38
	1727.22
	5.97765

	1727.82
	-14.5118
	1727.92
	-90.4728
	1727.85
	46.06999
	1727.85
	55.81665
	1727.85
	-2.70573
	1727.85
	24.18563
	1727.85
	-119.552
	1727.85
	7.05517

	1728.45
	-14.2904
	1728.55
	-91.0617
	1728.47
	43.68011
	1728.47
	55.39651
	1728.47
	-3.81349
	1728.47
	23.92877
	1728.47
	-119.287
	1728.47
	4.8898

	1729.08
	-14.0717
	1729.17
	-92.1546
	1729.1
	42.22749
	1729.1
	54.79611
	1729.1
	-4.0695
	1729.1
	23.49427
	1729.1
	-118.147
	1729.1
	3.66531

	1729.71
	-13.8562
	1729.8
	-93.0131
	1729.73
	44.17453
	1729.73
	55.60188
	1729.73
	-3.50544
	1729.73
	24.46595
	1729.73
	-116.187
	1729.73
	5.84048

	1730.33
	-13.6443
	1730.43
	-93.4888
	1730.36
	44.09259
	1730.36
	57.27619
	1730.36
	-3.47326
	1730.36
	26.30617
	1730.36
	-114.759
	1730.36
	5.98668

	1730.96
	-13.4359
	1731.06
	-93.1315
	1730.99
	43.06437
	1730.99
	57.01205
	1730.99
	-5.26813
	1730.99
	26.20794
	1730.99
	-115.159
	1730.99
	5.18659

	1731.59
	-13.2315
	1731.69
	-91.5447
	1731.62
	43.54561
	1731.62
	57.70331
	1731.62
	-4.29194
	1731.62
	27.06511
	1731.62
	-112.787
	1731.62
	5.89595

	1732.22
	-13.0297
	1732.32
	-93.1755
	1732.25
	44.51415
	1732.25
	56.66624
	1732.25
	-1.74901
	1732.25
	26.19395
	1732.25
	-108.848
	1732.25
	7.09262

	1732.84
	-12.8308
	1732.94
	-92.9
	1732.87
	44.07087
	1732.87
	58.23308
	1732.87
	-2.5415
	1732.87
	27.92407
	1732.87
	-108.267
	1732.87
	6.87385

	1733.47
	-12.6349
	1733.57
	-92.3981
	1733.5
	44.6465
	1733.5
	57.14316
	1733.5
	-2.35064
	1733.5
	27.00005
	1733.5
	-106.68
	1733.5
	7.67762

	1734.1
	-12.4422
	1734.2
	-92.4066
	1734.13
	46.65297
	1734.13
	54.22294
	1734.13
	-1.88323
	1734.13
	24.24575
	1734.13
	-104.817
	1734.13
	9.91222

	1734.72
	-12.2527
	1734.83
	-92.5299
	1734.76
	46.87556
	1734.76
	54.32263
	1734.76
	-0.74163
	1734.76
	24.51135
	1734.76
	-102.28
	1734.76
	10.36294

	1735.35
	-12.0665
	1735.46
	-93.6701
	1735.39
	47.50932
	1735.39
	54.92035
	1735.39
	0.46096
	1735.39
	25.27497
	1735.39
	-99.6818
	1735.39
	11.22483

	1735.98
	-11.8836
	1736.08
	-92.7841
	1736.02
	49.57341
	1736.02
	54.36422
	1736.02
	0.71289
	1736.02
	24.88475
	1736.02
	-98.0342
	1736.02
	13.51705

	1736.6
	-11.7038
	1736.71
	-93.6598
	1736.64
	49.49442
	1736.64
	53.75399
	1736.64
	-1.04515
	1736.64
	24.43779
	1736.64
	-98.4188
	1736.64
	13.66256

	1737.23
	-11.5272
	1737.34
	-94.252
	1737.27
	49.93834
	1737.27
	54.3552
	1737.27
	-1.22608
	1737.27
	25.20492
	1737.27
	-97.204
	1737.27
	14.33462

	1737.86
	-11.3535
	1737.97
	-94.0656
	1737.9
	50.32075
	1737.9
	56.13201
	1737.9
	-0.83281
	1737.9
	27.14763
	1737.9
	-95.4151
	1737.9
	14.94516

	1738.49
	-11.1827
	1738.59
	-96.3179
	1738.53
	51.88883
	1738.53
	55.69311
	1738.53
	-1.88992
	1738.53
	26.87464
	1738.53
	-95.0765
	1738.53
	16.74137

	1739.11
	-11.015
	1739.22
	-94.1161
	1739.16
	51.85775
	1739.16
	55.25451
	1739.16
	-1.43146
	1739.16
	26.60196
	1739.16
	-93.2223
	1739.16
	16.93841

	1739.74
	-10.8501
	1739.85
	-94.4408
	1739.78
	51.83798
	1739.78
	54.20551
	1739.78
	1.41256
	1739.78
	25.71623
	1739.78
	-89.0048
	1739.78
	17.14315

	1740.37
	-10.6883
	1740.48
	-94.5883
	1740.41
	53.87104
	1740.41
	54.86014
	1740.41
	0.83366
	1740.41
	26.53677
	1740.41
	-88.188
	1740.41
	19.40435

	1740.99
	-10.5296
	1741.1
	-94.6516
	1741.04
	53.77534
	1741.04
	55.56624
	1741.04
	-0.09125
	1741.04
	27.40878
	1741.04
	-87.7173
	1741.04
	19.53677

	1741.62
	-10.3741
	1741.73
	-93.8583
	1741.67
	54.35575
	1741.67
	54.65421
	1741.67
	-1.07824
	1741.67
	26.66266
	1741.67
	-87.3086
	1741.67
	20.34532

	1742.24
	-10.2223
	1742.36
	-93.8265
	1742.29
	54.67272
	1742.29
	56.61794
	1742.29
	-0.94051
	1742.29
	28.78966
	1742.29
	-85.7973
	1742.29
	20.8868

	1742.87
	-10.0743
	1742.99
	-93.7787
	1742.92
	54.57161
	1742.92
	56.31247
	1742.92
	0.44122
	1742.92
	28.6501
	1742.92
	-83.0199
	1742.92
	21.01382

	1743.5
	-9.93028
	1743.61
	-92.6163
	1743.55
	55.75401
	1743.55
	56.25365
	1743.55
	0.4665
	1743.55
	28.75719
	1743.55
	-81.599
	1743.55
	22.42435

	1744.12
	-9.79025
	1744.24
	-92.1838
	1744.18
	57.37391
	1744.18
	56.04474
	1744.18
	0.51067
	1744.18
	28.71418
	1744.18
	-80.1591
	1744.18
	24.27238

	1744.75
	-9.65448
	1744.87
	-93.1714
	1744.8
	58.60737
	1744.8
	55.69343
	1744.8
	1.17398
	1744.8
	28.52616
	1744.8
	-78.1223
	1744.8
	25.73035

	1745.37
	-9.52347
	1745.49
	-92.8342
	1745.43
	59.80112
	1745.43
	56.30203
	1745.43
	2.39632
	1745.43
	29.30066
	1745.43
	-75.5043
	1745.43
	27.15223

	1746
	-9.39722
	1746.12
	-92.1308
	1746.06
	60.08315
	1746.06
	57.8774
	1746.06
	3.02011
	1746.06
	31.04194
	1746.06
	-73.4848
	1746.06
	27.66239

	1746.63
	-9.2756
	1746.75
	-92.0979
	1746.68
	61.42801
	1746.68
	58.48617
	1746.68
	3.87764
	1746.68
	31.81399
	1746.68
	-71.2537
	1746.68
	29.23176

	1747.25
	-9.15858
	1747.37
	-92.45
	1747.31
	59.834
	1747.31
	58.60378
	1747.31
	10.43212
	1747.31
	32.09751
	1747.31
	-63.3036
	1747.31
	27.86588

	1747.88
	-9.04602
	1748
	-92.1925
	1747.94
	59.82821
	1747.94
	59.46177
	1747.94
	11.67465
	1747.94
	33.12141
	1747.94
	-60.6654
	1747.94
	28.08822

	1748.5
	-8.93778
	1748.63
	-94.2199
	1748.57
	59.34169
	1748.57
	60.54183
	1748.57
	14.1898
	1748.57
	34.36737
	1748.57
	-56.7546
	1748.57
	27.82983

	1749.13
	-8.83376
	1749.25
	-93.7353
	1749.19
	60.45161
	1749.19
	62.41585
	1749.19
	14.96402
	1749.19
	36.40467
	1749.19
	-54.6068
	1749.19
	29.16426

	1749.76
	-8.73356
	1749.88
	-94.1026
	1749.82
	63.1858
	1749.82
	63.58773
	1749.82
	15.26617
	1749.82
	37.74246
	1749.82
	-52.909
	1749.82
	32.12658

	1750.38
	-8.63726
	1750.51
	-94.1867
	1750.45
	64.42703
	1750.45
	65.99273
	1750.45
	17.25618
	1750.45
	40.31337
	1750.45
	-49.5233
	1750.45
	33.59594

	1751.01
	-8.54478
	1751.13
	-93.7153
	1751.07
	64.77586
	1751.07
	66.11577
	1751.07
	18.07567
	1751.07
	40.59968
	1751.07
	-47.3303
	1751.07
	34.16928

	1751.63
	-8.45602
	1751.76
	-93.6037
	1751.7
	67.4864
	1751.7
	66.11862
	1751.7
	16.96543
	1751.7
	40.76844
	1751.7
	-47.0448
	1751.7
	37.10795

	1752.26
	-8.37099
	1752.38
	-93.2814
	1752.33
	67.00399
	1752.33
	66.5895
	1752.33
	18.7309
	1752.33
	41.40523
	1752.33
	-43.8837
	1752.33
	36.85367

	1752.88
	-8.28963
	1753.01
	-95.3164
	1752.95
	68.31554
	1752.95
	67.8325
	1752.95
	19.49726
	1752.95
	42.81151
	1752.95
	-41.7438
	1752.95
	38.38973

	1753.51
	-8.21207
	1753.64
	-95.9363
	1753.58
	68.41835
	1753.58
	69.53128
	1753.58
	21.41561
	1753.58
	44.6762
	1753.58
	-38.4298
	1753.58
	38.72067

	1754.13
	-8.13792
	1754.26
	-95.9528
	1754.2
	70.18385
	1754.2
	70.59986
	1754.2
	23.83716
	1754.2
	45.90805
	1754.2
	-34.6347
	1754.2
	40.71068

	1754.76
	-8.0673
	1754.89
	-96.4136
	1754.83
	70.6271
	1754.83
	70.57805
	1754.83
	24.09991
	1754.83
	46.05215
	1754.83
	-32.9763
	1754.83
	41.38205

	1755.38
	-7.9995
	1755.52
	-95.5385
	1755.46
	70.98185
	1755.46
	70.9971
	1755.46
	25.11739
	1755.46
	46.63711
	1755.46
	-30.5631
	1755.46
	41.96494

	1756.01
	-7.9341
	1756.14
	-96.0086
	1756.08
	72.70106
	1756.08
	71.71752
	1756.08
	24.3983
	1756.08
	47.52081
	1756.08
	-29.9087
	1756.08
	43.90866

	1756.63
	-7.87043
	1756.77
	-95.9988
	1756.71
	73.89228
	1756.71
	72.0203
	1756.71
	24.83278
	1756.71
	47.98949
	1756.71
	-28.0785
	1756.71
	45.32801

	1757.26
	-7.80804
	1757.39
	-97.0553
	1757.34
	74.63782
	1757.34
	72.33876
	1757.34
	25.85752
	1757.34
	48.47387
	1757.34
	-25.6581
	1757.34
	46.30168

	1757.88
	-7.74678
	1758.02
	-97.7916
	1757.96
	75.46397
	1757.96
	72.55425
	1757.96
	27.44521
	1757.96
	48.85263
	1757.96
	-22.6969
	1757.96
	47.35234

	1758.51
	-7.68634
	1758.64
	-97.9552
	1758.59
	76.37931
	1758.59
	74.07546
	1758.59
	28.24381
	1758.59
	50.53975
	1758.59
	-20.5026
	1758.59
	48.49581

	1759.13
	-7.62669
	1759.27
	-97.658
	1759.21
	75.92605
	1759.21
	76.30566
	1759.21
	28.7138
	1759.21
	52.93322
	1759.21
	-18.6591
	1759.21
	48.26706

	1759.76
	-7.56719
	1759.9
	-97.7903
	1759.84
	76.23937
	1759.84
	77.71303
	1759.84
	28.63072
	1759.84
	54.5065
	1759.84
	-17.3465
	1759.84
	48.80851

	1760.38
	-7.50762
	1760.52
	-96.069
	1760.47
	78.17322
	1760.47
	79.32146
	1760.47
	27.71779
	1760.47
	56.28084
	1760.47
	-16.8638
	1760.47
	50.97049

	1761.01
	-7.44734
	1761.15
	-97.4559
	1761.09
	79.22931
	1761.09
	80.55253
	1761.09
	27.17524
	1761.09
	57.67518
	1761.09
	-16.0328
	1761.09
	52.25109

	1761.63
	-7.38606
	1761.77
	-96.7589
	1761.72
	77.93826
	1761.72
	79.64919
	1761.72
	25.74251
	1761.72
	56.93776
	1761.72
	-16.0698
	1761.72
	51.18817

	1762.25
	-7.32357
	1762.4
	-96.4163
	1762.34
	78.14214
	1762.34
	79.76701
	1762.34
	25.0803
	1762.34
	57.21885
	1762.34
	-15.3585
	1762.34
	51.61655

	1762.88
	-7.25962
	1763.02
	-95.5646
	1762.97
	79.40539
	1762.97
	78.73505
	1762.97
	25.62482
	1762.97
	56.3528
	1762.97
	-13.4183
	1762.97
	53.10794

	1763.5
	-7.19376
	1763.65
	-96.1863
	1763.59
	78.99908
	1763.59
	79.45364
	1763.59
	23.22908
	1763.59
	57.23467
	1763.59
	-14.4405
	1763.59
	52.92613

	1764.13
	-7.12582
	1764.27
	-95.5182
	1764.22
	79.11261
	1764.22
	79.21773
	1764.22
	20.72251
	1764.22
	57.16467
	1764.22
	-15.5514
	1764.22
	53.2678

	1764.75
	-7.05572
	1764.9
	-94.8481
	1764.84
	78.74956
	1764.84
	79.06543
	1764.84
	19.36358
	1764.84
	57.17564
	1764.84
	-15.5368
	1764.84
	53.12926

	1765.37
	-6.98329
	1765.52
	-93.5626
	1765.47
	78.89231
	1765.47
	79.62873
	1765.47
	16.80995
	1765.47
	57.90485
	1765.47
	-16.6948
	1765.47
	53.50014

	1766
	-6.90833
	1766.15
	-93.515
	1766.09
	77.44927
	1766.09
	79.70349
	1766.09
	15.00612
	1766.09
	58.14289
	1766.09
	-17.1251
	1766.09
	52.2816

	1766.62
	-6.83097
	1766.77
	-92.4208
	1766.72
	77.85921
	1766.72
	80.12472
	1766.72
	13.58812
	1766.72
	58.73003
	1766.72
	-17.1474
	1766.72
	52.91968

	1767.25
	-6.75098
	1767.4
	-92.8175
	1767.35
	78.72797
	1767.35
	79.74085
	1767.35
	11.61032
	1767.35
	58.51207
	1767.35
	-17.7296
	1767.35
	54.01657

	1767.87
	-6.66821
	1768.02
	-91.7072
	1767.97
	77.84703
	1767.97
	79.2904
	1767.97
	11.18761
	1767.97
	58.22489
	1767.97
	-16.7787
	1767.97
	53.36013

	1768.49
	-6.58276
	1768.65
	-91.3066
	1768.6
	78.14828
	1768.6
	79.8323
	1768.6
	9.10525
	1768.6
	58.9327
	1768.6
	-17.4654
	1768.6
	53.88952

	1769.12
	-6.49445
	1769.27
	-91.1115
	1769.22
	78.19374
	1769.22
	79.36624
	1769.22
	7.09092
	1769.22
	58.62992
	1769.22
	-18.1062
	1769.22
	54.15949

	1769.74
	-6.40318
	1769.89
	-91.6146
	1769.85
	77.48402
	1769.85
	78.28402
	1769.85
	7.78149
	1769.85
	57.71361
	1769.85
	-16.02
	1769.85
	53.6779

	1770.36
	-6.30845
	1770.52
	-90.7073
	1770.47
	76.57693
	1770.47
	78.41738
	1770.47
	6.72559
	1770.47
	58.01024
	1770.47
	-15.7024
	1770.47
	52.99532

	1770.99
	-6.21018
	1771.14
	-90.2308
	1771.09
	76.72744
	1771.09
	78.98729
	1771.09
	5.19905
	1771.09
	58.74342
	1771.09
	-15.8554
	1771.09
	53.37033

	1771.61
	-6.10842
	1771.77
	-90.4648
	1771.72
	76.74451
	1771.72
	80.27025
	1771.72
	4.33741
	1771.72
	60.19229
	1771.72
	-15.3213
	1771.72
	53.61554

	1772.24
	-6.00307
	1772.39
	-90.6869
	1772.34
	75.66364
	1772.34
	79.65506
	1772.34
	2.08871
	1772.34
	59.74038
	1772.34
	-16.1965
	1772.34
	52.75918

	1772.86
	-5.89431
	1773.02
	-91.8402
	1772.97
	76.45615
	1772.97
	78.75536
	1772.97
	0.24192
	1772.97
	59.00659
	1772.97
	-16.6476
	1772.97
	53.77982

	1773.48
	-5.78182
	1773.64
	-92.6048
	1773.59
	77.98718
	1773.59
	79.47731
	1773.59
	0.34497
	1773.59
	59.89182
	1773.59
	-15.6217
	1773.59
	55.53536

	1774.1
	-5.66561
	1774.27
	-92.8543
	1774.22
	78.06596
	1774.22
	79.20957
	1774.22
	1.63138
	1774.22
	59.78999
	1774.22
	-14.4459
	1774.22
	55.84227

	1774.73
	-5.54588
	1774.89
	-92.8096
	1774.84
	78.53831
	1774.84
	79.532
	1774.84
	1.72069
	1774.84
	60.27569
	1774.84
	-14.4655
	1774.84
	56.53912

	1775.35
	-5.42288
	1775.51
	-94.1538
	1775.47
	77.6567
	1775.47
	80.67936
	1775.47
	1.74259
	1775.47
	61.58896
	1775.47
	-14.5543
	1775.47
	55.88564

	1775.97
	-5.2966
	1776.14
	-94.4927
	1776.09
	76.84786
	1776.09
	80.7561
	1776.09
	4.28483
	1776.09
	61.82897
	1776.09
	-12.1209
	1776.09
	55.30132

	1776.6
	-5.16741
	1776.76
	-94.8825
	1776.71
	76.32015
	1776.71
	82.21135
	1776.71
	6.03507
	1776.71
	63.4475
	1776.71
	-10.4796
	1776.71
	54.99811

	1777.22
	-5.03564
	1777.39
	-96.2629
	1777.34
	75.8143
	1777.34
	82.18378
	1777.34
	8.01803
	1777.34
	63.58584
	1777.34
	-8.6073
	1777.34
	54.7204

	1777.84
	-4.90148
	1778.01
	-96.7974
	1777.96
	76.45717
	1777.96
	83.94982
	1777.96
	10.16415
	1777.96
	65.51515
	1777.96
	-6.57009
	1777.96
	55.58778

	1778.47
	-4.76489
	1778.63
	-96.7536
	1778.59
	75.9974
	1778.59
	83.2895
	1778.59
	10.12477
	1778.59
	65.02074
	1778.59
	-6.72014
	1778.59
	55.35614

	1779.09
	-4.62592
	1779.26
	-96.9437
	1779.21
	76.54806
	1779.21
	84.85817
	1779.21
	9.08749
	1779.21
	66.75269
	1779.21
	-7.86632
	1779.21
	56.1313

	1779.71
	-4.48471
	1779.88
	-96.506
	1779.83
	76.5544
	1779.83
	86.67174
	1779.83
	8.94904
	1779.83
	68.72953
	1779.83
	-8.11367
	1779.83
	56.36215

	1780.33
	-4.34141
	1780.5
	-96.6944
	1780.46
	78.57006
	1780.46
	86.5968
	1780.46
	10.23607
	1780.46
	68.8205
	1780.46
	-6.9373
	1780.46
	58.60595

	1780.96
	-4.19631
	1781.13
	-97.8719
	1781.08
	78.98209
	1781.08
	86.86017
	1781.08
	13.26233
	1781.08
	69.24715
	1781.08
	-4.01995
	1781.08
	59.24248

	1781.58
	-4.0498
	1781.75
	-97.46
	1781.71
	78.52809
	1781.71
	87.00394
	1781.71
	15.57342
	1781.71
	69.55683
	1781.71
	-1.81951
	1781.71
	59.01661

	1782.2
	-3.90185
	1782.37
	-97.2197
	1782.33
	78.94476
	1782.33
	86.03818
	1782.33
	16.79884
	1782.33
	68.75435
	1782.33
	-0.703
	1782.33
	59.65779

	1782.82
	-3.75288
	1783
	-96.6727
	1782.95
	79.53438
	1782.95
	88.09733
	1782.95
	18.41563
	1782.95
	70.97677
	1782.95
	0.80488
	1782.95
	60.47192

	1783.45
	-3.60299
	1783.62
	-97.0556
	1783.58
	79.45835
	1783.58
	88.61863
	1783.58
	19.65236
	1783.58
	71.66397
	1783.58
	1.93095
	1783.58
	60.62402

	1784.07
	-3.45227
	1784.24
	-96.7859
	1784.2
	80.00967
	1784.2
	89.47491
	1784.2
	20.98654
	1784.2
	72.68354
	1784.2
	3.15623
	1784.2
	61.39985

	1784.69
	-3.30118
	1784.87
	-95.4191
	1784.82
	80.08662
	1784.82
	89.27148
	1784.82
	20.86421
	1784.82
	72.64338
	1784.82
	2.92499
	1784.82
	61.70131

	1785.31
	-3.14995
	1785.49
	-95.0819
	1785.45
	80.78092
	1785.45
	88.23345
	1785.45
	21.32284
	1785.45
	71.77126
	1785.45
	3.27296
	1785.45
	62.62374

	1785.94
	-2.99933
	1786.11
	-96.1576
	1786.07
	80.51728
	1786.07
	88.35256
	1786.07
	21.23775
	1786.07
	72.05365
	1786.07
	3.07897
	1786.07
	62.58461

	1786.56
	-2.84935
	1786.74
	-96.6815
	1786.69
	81.05403
	1786.69
	89.7554
	1786.69
	22.34679
	1786.69
	73.61976
	1786.69
	4.0791
	1786.69
	63.34587

	1787.18
	-2.70043
	1787.36
	-96.9341
	1787.32
	82.0654
	1787.32
	90.12816
	1787.32
	26.3115
	1787.32
	74.15843
	1787.32
	7.93315
	1787.32
	64.58537

	1787.8
	-2.55237
	1787.98
	-96.0066
	1787.94
	82.28268
	1787.94
	90.57892
	1787.94
	27.57538
	1787.94
	74.77247
	1787.94
	9.08813
	1787.94
	65.02716

	1788.42
	-2.40534
	1788.6
	-96.0295
	1788.56
	82.89094
	1788.56
	90.91361
	1788.56
	31.68828
	1788.56
	75.27043
	1788.56
	13.09213
	1788.56
	65.85993

	1789.04
	-2.2589
	1789.23
	-97.2253
	1789.19
	82.24238
	1789.19
	91.16045
	1789.19
	33.54798
	1789.19
	75.68318
	1789.19
	14.84117
	1789.19
	65.4395

	1789.67
	-2.11293
	1789.85
	-98.8276
	1789.81
	83.1194
	1789.81
	92.62483
	1789.81
	34.64593
	1789.81
	77.31083
	1789.81
	15.83021
	1789.81
	66.54103

	1790.29
	-1.96756
	1790.47
	-98.7108
	1790.43
	84.6976
	1790.43
	93.76117
	1790.43
	35.64564
	1790.43
	78.61045
	1790.43
	16.72101
	1790.43
	68.34374

	1790.91
	-1.82299
	1791.1
	-97.5765
	1791.06
	85.93081
	1791.06
	95.03468
	1791.06
	36.95357
	1791.06
	80.04986
	1791.06
	17.91828
	1791.06
	69.80508

	1791.53
	-1.67973
	1791.72
	-98.0832
	1791.68
	86.33856
	1791.68
	95.05737
	1791.68
	38.05421
	1791.68
	80.23583
	1791.68
	18.91002
	1791.68
	70.43733

	1792.15
	-1.53757
	1792.34
	-98.8119
	1792.3
	87.19042
	1792.3
	95.82908
	1792.3
	41.43896
	1792.3
	81.17082
	1792.3
	22.18586
	1792.3
	71.51371

	1792.77
	-1.39632
	1792.96
	-98.8426
	1792.92
	87.79935
	1792.92
	96.15982
	1792.92
	44.52528
	1792.92
	81.66483
	1792.92
	25.16328
	1792.92
	72.34714

	1793.4
	-1.25584
	1793.58
	-97.8348
	1793.55
	88.83988
	1793.55
	97.79702
	1793.55
	48.66899
	1793.55
	83.46795
	1793.55
	29.19633
	1793.55
	73.61581

	1794.02
	-1.11612
	1794.21
	-97.755
	1794.17
	87.99542
	1794.17
	98.7396
	1794.17
	50.74741
	1794.17
	84.5738
	1794.17
	31.16585
	1794.17
	72.99585

	1794.64
	-0.97711
	1794.83
	-98.3488
	1794.79
	87.97442
	1794.79
	102.0433
	1794.79
	54.045
	1794.79
	88.04072
	1794.79
	34.35453
	1794.79
	73.19936

	1795.26
	-0.83869
	1795.45
	-98.7896
	1795.41
	89.29505
	1795.41
	104.1356
	1795.41
	57.45597
	1795.41
	90.29638
	1795.41
	37.6566
	1795.41
	74.7445

	1795.88
	-0.70082
	1796.07
	-97.438
	1796.04
	91.01696
	1796.04
	107.7354
	1796.04
	60.05144
	1796.04
	94.06204
	1796.04
	40.14141
	1796.04
	76.69454

	1796.5
	-0.56348
	1796.69
	-96.3702
	1796.66
	92.49851
	1796.66
	108.4912
	1796.66
	64.76922
	1796.66
	94.98112
	1796.66
	44.75029
	1796.66
	78.4006

	1797.12
	-0.42681
	1797.32
	-95.8564
	1797.28
	93.7528
	1797.28
	110.4893
	1797.28
	70.21014
	1797.28
	97.14255
	1797.28
	50.0823
	1797.28
	79.87941

	1797.74
	-0.2907
	1797.94
	-95.9547
	1797.9
	95.499
	1797.9
	113.0707
	1797.9
	75.29532
	1797.9
	99.8872
	1797.9
	55.05857
	1797.9
	81.85011

	1798.36
	-0.15516
	1798.56
	-96.1949
	1798.53
	97.08177
	1798.53
	114.1499
	1798.53
	79.49421
	1798.53
	101.1322
	1798.53
	59.1468
	1798.53
	83.66101

	1798.99
	-0.0206
	1799.18
	-95.5837
	1799.15
	98.09267
	1799.15
	115.073
	1799.15
	85.20351
	1799.15
	102.2187
	1799.15
	64.7472
	1799.15
	84.89642

	1799.61
	0.11304
	1799.8
	-95.4446
	1799.77
	100.0059
	1799.77
	118.7297
	1799.77
	89.1204
	1799.77
	106.0387
	1799.77
	68.55518
	1799.77
	87.03413

	1800.23
	0.24572
	1800.43
	-95.8806
	1800.39
	101.0271
	1800.39
	120.7428
	1800.39
	95.22552
	1800.39
	108.215
	1800.39
	74.5514
	1800.39
	88.27987

	1800.85
	0.37708
	1801.05
	-95.6894
	1801.01
	103.4801
	1801.01
	123.2034
	1801.01
	100.8583
	1801.01
	110.8389
	1801.01
	80.07526
	1801.01
	90.95738

	1801.47
	0.5071
	1801.67
	-95.014
	1801.64
	105.7318
	1801.64
	125.2349
	1801.64
	104.2765
	1801.64
	113.0363
	1801.64
	83.3828
	1801.64
	93.43718

	1802.09
	0.63595
	1802.29
	-94.7178
	1802.26
	108.0049
	1802.26
	126.5445
	1802.26
	108.5045
	1802.26
	114.5092
	1802.26
	87.5019
	1802.26
	95.93483

	1802.71
	0.76367
	1802.91
	-95.0559
	1802.88
	110.0186
	1802.88
	128.3842
	1802.88
	112.5713
	1802.88
	116.5122
	1802.88
	91.45983
	1802.88
	98.17306

	1803.33
	0.89025
	1803.53
	-95.1408
	1803.5
	113.1298
	1803.5
	130.71
	1803.5
	115.8395
	1803.5
	119.0012
	1803.5
	94.61908
	1803.5
	101.5087

	1803.95
	1.01557
	1804.15
	-95.8349
	1804.12
	114.6338
	1804.12
	133.2712
	1804.12
	122.5327
	1804.12
	121.7257
	1804.12
	101.2034
	1804.12
	103.2373

	1804.57
	1.13972
	1804.78
	-96.1397
	1804.74
	116.2914
	1804.74
	136.9236
	1804.74
	129.1668
	1804.74
	125.5414
	1804.74
	107.7286
	1804.74
	105.1194

	1805.19
	1.26235
	1805.4
	-96.2324
	1805.36
	117.5917
	1805.36
	139.1896
	1805.36
	133.2204
	1805.36
	127.9707
	1805.36
	111.6732
	1805.36
	106.6441

	1805.81
	1.38356
	1806.02
	-97.6356
	1805.99
	120.5301
	1805.99
	140.2785
	1805.99
	135.9775
	1805.99
	129.2255
	1805.99
	114.3197
	1805.99
	109.8107

	1806.43
	1.50327
	1806.64
	-97.1632
	1806.61
	123.008
	1806.61
	142.819
	1806.61
	139.641
	1806.61
	131.9293
	1806.61
	117.8744
	1806.61
	112.5131

	1807.05
	1.62127
	1807.26
	-97.6287
	1807.23
	125.2704
	1807.23
	145.1604
	1807.23
	144.0003
	1807.23
	134.434
	1807.23
	122.1247
	1807.23
	115

	1807.67
	1.73734
	1807.88
	-98.0155
	1807.85
	127.9804
	1807.85
	146.6152
	1807.85
	146.9499
	1807.85
	136.052
	1807.85
	124.9654
	1807.85
	117.9345

	1808.29
	1.85137
	1808.5
	-97.9213
	1808.47
	129.5751
	1808.47
	148.6132
	1808.47
	150.2767
	1808.47
	138.2133
	1808.47
	128.1833
	1808.47
	119.7537

	1808.91
	1.9632
	1809.12
	-99.1706
	1809.09
	130.9722
	1809.09
	152.1154
	1809.09
	151.2342
	1809.09
	141.8787
	1809.09
	129.0319
	1809.09
	121.3753

	1809.53
	2.07257
	1809.74
	-99.6332
	1809.71
	130.9429
	1809.71
	151.9622
	1809.71
	153.8071
	1809.71
	141.8888
	1809.71
	131.4959
	1809.71
	121.5706

	1810.15
	2.17924
	1810.36
	-99.9926
	1810.33
	130.7448
	1810.33
	153.8995
	1810.33
	157.0757
	1810.33
	143.9894
	1810.33
	134.6556
	1810.33
	121.597

	1810.77
	2.28329
	1810.98
	-99.9109
	1810.96
	132.0227
	1810.96
	154.4727
	1810.96
	160.2354
	1810.96
	144.7285
	1810.96
	137.7046
	1810.96
	123.103

	1811.39
	2.38465
	1811.61
	-100.802
	1811.58
	133.9601
	1811.58
	154.4034
	1811.58
	162.6465
	1811.58
	144.8225
	1811.58
	140.0069
	1811.58
	125.2649

	1812.01
	2.48368
	1812.23
	-101.445
	1812.2
	135.371
	1812.2
	155.83
	1812.2
	164.5705
	1812.2
	146.4124
	1812.2
	141.822
	1812.2
	126.9003

	1812.63
	2.58052
	1812.85
	-99.6474
	1812.82
	136.8397
	1812.82
	157.2251
	1812.82
	166.7185
	1812.82
	147.9708
	1812.82
	143.861
	1812.82
	128.5936

	1813.25
	2.67481
	1813.47
	-99.3049
	1813.44
	138.0934
	1813.44
	158.282
	1813.44
	168.3803
	1813.44
	149.1909
	1813.44
	145.4139
	1813.44
	130.0717

	1813.87
	2.76636
	1814.09
	-99.3305
	1814.06
	138.6603
	1814.06
	160.2633
	1814.06
	170.1643
	1814.06
	151.3355
	1814.06
	147.0891
	1814.06
	130.8632

	1814.49
	2.85543
	1814.71
	-98.7176
	1814.68
	139.1776
	1814.68
	158.9918
	1814.68
	172.9557
	1814.68
	150.2273
	1814.68
	149.7716
	1814.68
	131.605

	1815.11
	2.94185
	1815.33
	-98.2413
	1815.3
	139.528
	1815.3
	160.4987
	1815.3
	175.9165
	1815.3
	151.8974
	1815.3
	152.6234
	1815.3
	132.1798

	1815.73
	3.02573
	1815.95
	-97.2811
	1815.92
	140.4262
	1815.92
	162.2694
	1815.92
	178.462
	1815.92
	153.8314
	1815.92
	155.06
	1815.92
	133.3025

	1816.35
	3.10742
	1816.57
	-97.3437
	1816.54
	142.0805
	1816.54
	162.8204
	1816.54
	181.4092
	1816.54
	154.5456
	1816.54
	157.8983
	1816.54
	135.1813

	1816.96
	3.18678
	1817.19
	-97.0391
	1817.16
	143.1087
	1817.16
	165.0127
	1817.16
	183.8835
	1817.16
	156.9012
	1817.16
	160.2637
	1817.16
	136.4341

	1817.58
	3.26394
	1817.81
	-96.5069
	1817.78
	143.5676
	1817.78
	166.467
	1817.78
	186.1909
	1817.78
	158.5189
	1817.78
	162.4622
	1817.78
	137.1175

	1818.2
	3.33855
	1818.43
	-96.0382
	1818.4
	144.4846
	1818.4
	166.5722
	1818.4
	189.2567
	1818.4
	158.7873
	1818.4
	165.4191
	1818.4
	138.259

	1818.82
	3.41068
	1819.05
	-95.1406
	1819.02
	144.8888
	1819.02
	166.7218
	1819.02
	189.8766
	1819.02
	159.1002
	1819.02
	165.9301
	1819.02
	138.8877

	1819.44
	3.48033
	1819.67
	-96.7451
	1819.64
	146.2487
	1819.64
	167.4401
	1819.64
	191.6875
	1819.64
	159.9818
	1819.64
	167.6321
	1819.64
	140.4721

	1820.06
	3.54781
	1820.29
	-97.3505
	1820.26
	147.2196
	1820.26
	167.4693
	1820.26
	192.7926
	1820.26
	160.1743
	1820.26
	168.6282
	1820.26
	141.6675

	1820.68
	3.61342
	1820.91
	-96.4666
	1820.88
	148.9628
	1820.88
	167.8589
	1820.88
	196.0462
	1820.88
	160.7271
	1820.88
	171.7729
	1820.88
	143.6352

	1821.3
	3.67745
	1821.53
	-96.65
	1821.5
	150.1544
	1821.5
	168.6739
	1821.5
	197.379
	1821.5
	161.7054
	1821.5
	172.9968
	1821.5
	145.0514

	1821.92
	3.74026
	1822.15
	-96.7289
	1822.12
	149.536
	1822.12
	168.4418
	1822.12
	199.5664
	1822.12
	161.6365
	1822.12
	175.0754
	1822.12
	144.6574

	1822.53
	3.80208
	1822.76
	-96.9437
	1822.74
	149.2981
	1822.74
	168.8563
	1822.74
	201.9455
	1822.74
	162.2143
	1822.74
	177.3455
	1822.74
	144.6441

	1823.15
	3.86283
	1823.39
	-96.4887
	1823.36
	149.7371
	1823.36
	170.3604
	1823.36
	204.5037
	1823.36
	163.8817
	1823.36
	179.7949
	1823.36
	145.3076

	1823.77
	3.92231
	1824
	-97.2756
	1823.98
	149.7416
	1823.98
	171.4167
	1823.98
	205.5563
	1823.98
	165.1013
	1823.98
	180.7385
	1823.98
	145.5366

	1824.39
	3.9808
	1824.62
	-96.4464
	1824.6
	151.2166
	1824.6
	171.5419
	1824.6
	206.4731
	1824.6
	165.3898
	1824.6
	181.5464
	1824.6
	147.2361

	1825.01
	4.0383
	1825.24
	-96.4453
	1825.22
	150.2791
	1825.22
	171.3777
	1825.22
	208.3703
	1825.22
	165.3888
	1825.22
	183.3347
	1825.22
	146.5231

	1825.63
	4.09504
	1825.86
	-97.1019
	1825.84
	152.1524
	1825.84
	170.9601
	1825.84
	210.1332
	1825.84
	165.1345
	1825.84
	184.9887
	1825.84
	148.6209

	1826.24
	4.15119
	1826.48
	-96.665
	1826.46
	153.8066
	1826.46
	170.6114
	1826.46
	210.3322
	1826.46
	164.9491
	1826.46
	185.0788
	1826.46
	150.4997

	1826.86
	4.20679
	1827.1
	-95.9987
	1827.08
	154.8043
	1827.08
	170.3296
	1827.08
	212.2688
	1827.08
	164.8306
	1827.08
	186.9065
	1827.08
	151.7219

	1827.48
	4.26202
	1827.72
	-96.6592
	1827.7
	155.6791
	1827.7
	168.7963
	1827.7
	214.9794
	1827.7
	163.4606
	1827.7
	189.5082
	1827.7
	152.8211

	1828.1
	4.31682
	1828.34
	-97.4304
	1828.32
	157.0046
	1828.32
	169.0742
	1828.32
	215.4977
	1828.32
	163.9018
	1828.32
	189.9176
	1828.32
	154.3711

	1828.72
	4.37133
	1828.96
	-98.8054
	1828.94
	157.3195
	1828.94
	169.92
	1828.94
	214.3828
	1828.94
	164.9108
	1828.94
	188.6938
	1828.94
	154.9105

	1829.33
	4.42553
	1829.58
	-98.4084
	1829.56
	157.0734
	1829.56
	171.2604
	1829.56
	215.2976
	1829.56
	166.4145
	1829.56
	189.4997
	1829.56
	154.889

	1829.95
	4.47963
	1830.19
	-96.8502
	1830.18
	157.3459
	1830.18
	172.1341
	1830.18
	216.5527
	1830.18
	167.4515
	1830.18
	190.6459
	1830.18
	155.386

	1830.57
	4.53353
	1830.81
	-95.8739
	1830.79
	157.1744
	1830.79
	171.8549
	1830.79
	215.9327
	1830.79
	167.3329
	1830.79
	189.9187
	1830.79
	155.4353

	1831.19
	4.58697
	1831.43
	-96.9944
	1831.41
	157.5618
	1831.41
	171.3515
	1831.41
	215.9983
	1831.41
	166.9928
	1831.41
	189.8755
	1831.41
	156.0472

	1831.81
	4.63977
	1832.05
	-95.9823
	1832.03
	158.3946
	1832.03
	170.8464
	1832.03
	215.3332
	1832.03
	166.6509
	1832.03
	189.1015
	1832.03
	157.1046

	1832.42
	4.69173
	1832.67
	-95.735
	1832.65
	157.3239
	1832.65
	170.2331
	1832.65
	215.3632
	1832.65
	166.2009
	1832.65
	189.0225
	1832.65
	156.2584

	1833.04
	4.74272
	1833.29
	-94.9311
	1833.27
	157.7125
	1833.27
	169.4341
	1833.27
	216.0682
	1833.27
	165.5652
	1833.27
	189.6186
	1833.27
	156.8715

	1833.66
	4.79265
	1833.91
	-95.1197
	1833.89
	156.8084
	1833.89
	171.2159
	1833.89
	217.1799
	1833.89
	167.5103
	1833.89
	190.6214
	1833.89
	156.1919

	1834.28
	4.84191
	1834.52
	-95.1775
	1834.51
	155.9607
	1834.51
	170.0432
	1834.51
	217.2351
	1834.51
	166.5008
	1834.51
	190.5678
	1834.51
	155.5687

	1834.89
	4.89101
	1835.14
	-94.4574
	1835.13
	155.0987
	1835.13
	169.898
	1835.13
	216.1027
	1835.13
	166.5189
	1835.13
	189.3264
	1835.13
	154.9313

	1835.51
	4.94055
	1835.76
	-92.7884
	1835.75
	153.836
	1835.75
	169.4283
	1835.75
	214.7478
	1835.75
	166.2125
	1835.75
	187.8627
	1835.75
	153.893

	1836.13
	4.99075
	1836.38
	-93.2358
	1836.36
	153.1859
	1836.36
	168.004
	1836.36
	213.7344
	1836.36
	164.9488
	1836.36
	186.7421
	1836.36
	153.4639

	1836.75
	5.03964
	1837
	-94.5449
	1836.98
	152.4275
	1836.98
	167.0868
	1836.98
	214.9703
	1836.98
	164.1949
	1836.98
	187.8691
	1836.98
	152.9299

	1837.36
	5.08612
	1837.62
	-95.1126
	1837.6
	151.3806
	1837.6
	167.4617
	1837.6
	215.0225
	1837.6
	164.733
	1837.6
	187.8123
	1837.6
	152.1075

	1837.98
	5.13026
	1838.23
	-94.7797
	1838.22
	150.3488
	1838.22
	166.6922
	1838.22
	215.9715
	1838.22
	164.1269
	1838.22
	188.6525
	1838.22
	151.3002

	1838.6
	5.17404
	1838.85
	-94.7383
	1838.84
	150.095
	1838.84
	165.9981
	1838.84
	216.0572
	1838.84
	163.5961
	1838.84
	188.6293
	1838.84
	151.271

	1839.21
	5.21577
	1839.47
	-95.0121
	1839.46
	149.3184
	1839.46
	167.1443
	1839.46
	215.6509
	1839.46
	164.9055
	1839.46
	188.1141
	1839.46
	150.7189

	1839.83
	5.25538
	1840.09
	-96.4065
	1840.07
	149.7243
	1840.07
	166.556
	1840.07
	217.2438
	1840.07
	164.4779
	1840.07
	189.5998
	1840.07
	151.3457

	1840.45
	5.29361
	1840.71
	-96.9582
	1840.69
	150.5915
	1840.69
	165.4055
	1840.69
	220.1193
	1840.69
	163.4907
	1840.69
	192.3664
	1840.69
	152.4373

	1841.06
	5.33157
	1841.32
	-96.5452
	1841.31
	151.868
	1841.31
	165.4394
	1841.31
	220.6867
	1841.31
	163.6878
	1841.31
	192.8249
	1841.31
	153.9384

	1841.68
	5.36613
	1841.94
	-95.936
	1841.93
	153.0766
	1841.93
	165.3676
	1841.93
	221.8707
	1841.93
	163.7793
	1841.93
	193.9
	1841.93
	155.3715

	1842.3
	5.39124
	1842.56
	-96.8851
	1842.55
	153.4809
	1842.55
	166.1139
	1842.55
	222.8176
	1842.55
	164.6889
	1842.55
	194.738
	1842.55
	156.0003

	1842.91
	5.40621
	1843.18
	-96.8256
	1843.16
	153.5832
	1843.16
	166.0445
	1843.16
	224.4083
	1843.16
	164.7801
	1843.16
	196.2215
	1843.16
	156.3234

	1843.53
	5.41173
	1843.79
	-96.8311
	1843.78
	153.1363
	1843.78
	166.8126
	1843.78
	226.7274
	1843.78
	165.7114
	1843.78
	198.4317
	1843.78
	156.1011

	1844.15
	5.41378
	1844.41
	-96.6838
	1844.4
	153.0491
	1844.4
	166.7725
	1844.4
	228.3093
	1844.4
	165.8347
	1844.4
	199.9047
	1844.4
	156.2384

	1844.76
	5.41262
	1845.03
	-96.7571
	1845.02
	153.19
	1845.02
	167.0393
	1845.02
	229.2393
	1845.02
	166.2647
	1845.02
	200.7258
	1845.02
	156.6039

	1845.38
	5.40566
	1845.65
	-97.9994
	1845.63
	152.4281
	1845.63
	166.5632
	1845.63
	229.6401
	1845.63
	165.9493
	1845.63
	201.0195
	1845.63
	156.0628

	1846
	5.39457
	1846.26
	-97.5927
	1846.25
	152.1799
	1846.25
	167.5033
	1846.25
	230.3757
	1846.25
	167.0526
	1846.25
	201.6462
	1846.25
	156.0391

	1846.61
	5.37301
	1846.88
	-96.4553
	1846.87
	152.3077
	1846.87
	167.6585
	1846.87
	230.965
	1846.87
	167.3711
	1846.87
	202.1265
	1846.87
	156.3914

	1847.23
	5.3263
	1847.5
	-96.433
	1847.49
	152.4666
	1847.49
	167.3471
	1847.49
	231.1612
	1847.49
	167.223
	1847.49
	202.2138
	1847.49
	156.7748

	1847.84
	5.24206
	1848.11
	-96.6355
	1848.1
	151.2357
	1848.1
	168.3669
	1848.1
	232.7759
	1848.1
	168.4034
	1848.1
	203.7214
	1848.1
	155.7648

	1848.46
	5.24921
	1848.73
	-97.2465
	1848.72
	150.4062
	1848.72
	167.6026
	1848.72
	233.025
	1848.72
	167.8024
	1848.72
	203.8616
	1848.72
	155.1598

	1849.08
	5.25763
	1849.35
	-96.9137
	1849.34
	151.8142
	1849.34
	168.3617
	1849.34
	233.4963
	1849.34
	168.7248
	1849.34
	204.224
	1849.34
	156.7924

	1849.69
	5.26649
	1849.97
	-96.4467
	1849.96
	152.3364
	1849.96
	168.021
	1849.96
	232.8072
	1849.96
	168.5474
	1849.96
	203.426
	1849.96
	157.539

	1850.31
	5.27648
	1850.58
	-96.3716
	1850.57
	152.8293
	1850.57
	168.7232
	1850.57
	233.9813
	1850.57
	169.4103
	1850.57
	204.493
	1850.57
	158.2529

	1850.92
	5.28908
	1851.2
	-96.4162
	1851.19
	152.4393
	1851.19
	168.5589
	1851.19
	235.4759
	1851.19
	169.4092
	1851.19
	205.8786
	1851.19
	158.0873

	1851.54
	5.30449
	1851.82
	-96.2843
	1851.81
	152.4891
	1851.81
	169.071
	1851.81
	235.1407
	1851.81
	170.0845
	1851.81
	205.4346
	1851.81
	158.3617

	1852.16
	5.32333
	1852.43
	-95.5052
	1852.42
	151.5406
	1852.42
	169.4769
	1852.42
	235.8802
	1852.42
	170.6511
	1852.42
	206.0669
	1852.42
	157.634

	1852.77
	5.3462
	1853.05
	-95.4896
	1853.04
	151.0085
	1853.04
	167.7662
	1853.04
	237.6315
	1853.04
	169.1037
	1853.04
	207.7093
	1853.04
	157.3264

	1853.39
	5.3737
	1853.67
	-94.8
	1853.66
	151.1595
	1853.66
	167.1482
	1853.66
	238.3835
	1853.66
	168.649
	1853.66
	208.3524
	1853.66
	157.702

	1854
	5.4072
	1854.28
	-93.4835
	1854.28
	151.6241
	1854.28
	167.005
	1854.28
	238.2015
	1854.28
	168.669
	1854.28
	208.0615
	1854.28
	158.3911

	1854.62
	5.44789
	1854.9
	-92.8421
	1854.89
	151.3042
	1854.89
	166.6821
	1854.89
	235.8758
	1854.89
	168.5067
	1854.89
	205.6286
	1854.89
	158.2921

	1855.23
	5.49696
	1855.51
	-92.2039
	1855.51
	151.4948
	1855.51
	165.3122
	1855.51
	235.9923
	1855.51
	167.3002
	1855.51
	205.6363
	1855.51
	158.7072

	1855.85
	5.55417
	1856.13
	-92.7864
	1856.13
	150.8146
	1856.13
	165.4614
	1856.13
	236.8087
	1856.13
	167.6126
	1856.13
	206.3438
	1856.13
	158.2515

	1856.46
	5.62007
	1856.75
	-93.2946
	1856.74
	152.0743
	1856.74
	165.266
	1856.74
	236.141
	1856.74
	167.5778
	1856.74
	205.5689
	1856.74
	159.7321

	1857.08
	5.69441
	1857.36
	-93.019
	1857.36
	151.9688
	1857.36
	165.8403
	1857.36
	237.6315
	1857.36
	168.3155
	1857.36
	206.9505
	1857.36
	159.8511

	1857.7
	5.7785
	1857.98
	-93.0706
	1857.97
	150.6024
	1857.97
	166.1987
	1857.97
	238.1267
	1857.97
	168.8345
	1857.97
	207.3385
	1857.97
	158.7056

	1858.31
	5.87386
	1858.6
	-92.7021
	1858.59
	149.4211
	1858.59
	165.7762
	1858.59
	238.7504
	1858.59
	168.5753
	1858.59
	207.8533
	1858.59
	157.7488

	1858.93
	5.98129
	1859.21
	-92.809
	1859.21
	147.7258
	1859.21
	166.2241
	1859.21
	238.0652
	1859.21
	169.1865
	1859.21
	207.0592
	1859.21
	156.2779

	1859.54
	6.10137
	1859.83
	-92.3489
	1859.82
	147.0707
	1859.82
	166.1883
	1859.82
	236.3405
	1859.82
	169.3112
	1859.82
	205.2274
	1859.82
	155.8437

	1860.16
	6.23469
	1860.44
	-93.3176
	1860.44
	147.0443
	1860.44
	164.8113
	1860.44
	237.743
	1860.44
	168.0976
	1860.44
	206.521
	1860.44
	156.0419

	1860.17
	6.3824
	1861.06
	-93.8798
	1861.06
	147.4545
	1861.06
	162.5949
	1861.06
	236.4552
	1861.06
	166.0444
	1861.06
	205.1242
	1861.06
	156.6766

	1860.78
	6.54502
	1861.68
	-94.4579
	1861.67
	147.2848
	1861.67
	162.2444
	1861.67
	235.0812
	1861.67
	165.8545
	1861.67
	203.6431
	1861.67
	156.7278

	1861.4
	6.72211
	1862.29
	-94.6828
	1862.29
	146.3662
	1862.29
	162.4656
	1862.29
	235.0184
	1862.29
	166.239
	1862.29
	203.4714
	1862.29
	156.0337

	1862.02
	6.91447
	1862.91
	-93.9276
	1862.9
	145.1367
	1862.9
	160.6924
	1862.9
	234.6034
	1862.9
	164.6265
	1862.9
	202.9493
	1862.9
	155.0251

	1862.63
	7.12307
	1863.52
	-94.332
	1863.52
	143.7078
	1863.52
	159.8476
	1863.52
	233.4055
	1863.52
	163.945
	1863.52
	201.6424
	1863.52
	153.8207

	1863.25
	7.34808
	1864.14
	-94.2799
	1864.14
	143.4096
	1864.14
	159.3081
	1864.14
	231.1301
	1864.14
	163.5687
	1864.14
	199.2582
	1864.14
	153.747

	1863.87
	7.59019
	1864.75
	-95.1385
	1864.75
	143.0732
	1864.75
	159.8318
	1864.75
	228.3443
	1864.75
	164.2531
	1864.75
	196.3652
	1864.75
	153.6314

	1864.48
	7.84947
	1865.37
	-95.0886
	1865.37
	142.0031
	1865.37
	157.7523
	1865.37
	226.6875
	1865.37
	162.3369
	1865.37
	194.5995
	1865.37
	152.7859

	1865.1
	8.12629
	1865.98
	-94.6893
	1865.98
	141.4717
	1865.98
	156.1712
	1865.98
	224.4411
	1865.98
	160.9164
	1865.98
	192.2459
	1865.98
	152.4754

	1865.72
	8.42116
	1866.6
	-94.8863
	1866.6
	140.7494
	1866.6
	154.6622
	1866.6
	223.2407
	1866.6
	159.5707
	1866.6
	190.9367
	1866.6
	151.9776

	1866.33
	8.73432
	1867.21
	-94.5825
	1867.21
	140.7659
	1867.21
	152.3155
	1867.21
	221.9639
	1867.21
	157.3846
	1867.21
	189.5527
	1867.21
	152.2149

	1866.95
	9.06475
	1867.83
	-94.4127
	1867.83
	140.6124
	1867.83
	151.0385
	1867.83
	221.1137
	1867.83
	156.2709
	1867.83
	188.5936
	1867.83
	152.286

	1867.56
	9.41178
	1868.44
	-93.8709
	1868.44
	139.8386
	1868.44
	150.7563
	1868.44
	219.5492
	1868.44
	156.1493
	1868.44
	186.9219
	1868.44
	151.7331

	1868.18
	9.7739
	1869.06
	-94.3498
	1869.06
	138.6467
	1869.06
	149.6659
	1869.06
	219.175
	1869.06
	155.2223
	1869.06
	186.4389
	1869.06
	150.7657

	1868.8
	10.15038
	1869.67
	-94.8471
	1869.68
	137.3665
	1869.68
	148.5714
	1869.68
	215.8862
	1869.68
	154.291
	1869.68
	183.0411
	1869.68
	149.71

	1869.41
	10.54181
	1870.29
	-94.2659
	1870.29
	135.961
	1870.29
	146.946
	1870.29
	213.0078
	1870.29
	152.8262
	1870.29
	180.0556
	1870.29
	148.5254

	1870.03
	10.94869
	1870.9
	-94.6483
	1870.91
	133.981
	1870.91
	145.5814
	1870.91
	212.2872
	1870.91
	151.625
	1870.91
	179.226
	1870.91
	146.7699

	1870.64
	11.37054
	1871.52
	-94.3146
	1871.52
	132.3218
	1871.52
	144.6696
	1871.52
	208.4086
	1871.52
	150.8737
	1871.52
	175.2403
	1871.52
	145.3316

	1871.26
	11.80505
	1872.14
	-94.8549
	1872.14
	130.7082
	1872.14
	142.5788
	1872.14
	206.2891
	1872.14
	148.9463
	1872.14
	173.0119
	1872.14
	143.9425

	1871.87
	12.25063
	1872.75
	-95.0528
	1872.75
	129.321
	1872.75
	141.7243
	1872.75
	204.5768
	1872.75
	148.2523
	1872.75
	171.1925
	1872.75
	142.7761

	1872.49
	12.70568
	1873.36
	-95.0501
	1873.37
	128.1167
	1873.37
	140.3628
	1873.37
	200.7319
	1873.37
	147.0541
	1873.37
	167.2387
	1873.37
	141.7964

	1873.11
	13.16981
	1873.98
	-94.9575
	1873.98
	125.8161
	1873.98
	139.2661
	1873.98
	197.4989
	1873.98
	146.118
	1873.98
	163.8985
	1873.98
	139.7167

	1873.72
	13.64233
	1874.59
	-95.6365
	1874.6
	123.4819
	1874.6
	138.2956
	1874.6
	194.9801
	1874.6
	145.3108
	1874.6
	161.2708
	1874.6
	137.607

	1874.34
	14.1228
	1875.21
	-96.7888
	1875.21
	121.3842
	1875.21
	136.7312
	1875.21
	190.2354
	1875.21
	143.9071
	1875.21
	156.4189
	1875.21
	135.7301

	1874.95
	14.61065
	1875.82
	-96.3712
	1875.83
	119.4825
	1875.83
	134.3917
	1875.83
	184.8466
	1875.83
	141.7308
	1875.83
	150.9212
	1875.83
	134.0529

	1875.57
	15.10523
	1876.44
	-96.6885
	1876.44
	117.7112
	1876.44
	131.9639
	1876.44
	181.7001
	1876.44
	139.4637
	1876.44
	147.6676
	1876.44
	132.5025

	1876.18
	15.60555
	1877.05
	-96.3476
	1877.05
	116.5036
	1877.05
	130.0476
	1877.05
	180.1245
	1877.05
	137.7081
	1877.05
	145.9849
	1877.05
	131.5158

	1876.8
	16.11206
	1877.67
	-96.084
	1877.67
	115.5208
	1877.67
	127.6266
	1877.67
	176.7623
	1877.67
	135.4503
	1877.67
	142.5138
	1877.67
	130.7576

	1877.41
	16.62397
	1878.28
	-95.416
	1878.28
	114.0303
	1878.28
	125.4468
	1878.28
	174.035
	1878.28
	133.4312
	1878.28
	139.6793
	1878.28
	129.4879

	1878.03
	17.13952
	1878.89
	-95.3489
	1878.9
	111.1667
	1878.9
	123.7184
	1878.9
	172.5402
	1878.9
	131.8661
	1878.9
	138.0756
	1878.9
	126.8489

	1878.64
	17.65977
	1879.51
	-96.6118
	1879.51
	110.1745
	1879.51
	120.8369
	1879.51
	169.4067
	1879.51
	129.1452
	1879.51
	134.835
	1879.51
	126.0776

	1879.26
	18.18431
	1880.12
	-97.3365
	1880.13
	108.5569
	1880.13
	118.7816
	1880.13
	166.9629
	1880.13
	127.2532
	1880.13
	132.2822
	1880.13
	124.6845

	1879.87
	18.71232
	1880.74
	-98.1739
	1880.74
	105.6242
	1880.74
	116.444
	1880.74
	163.8429
	1880.74
	125.0762
	1880.74
	129.0551
	1880.74
	121.9726

	1880.49
	19.24339
	1881.35
	-97.5977
	1881.36
	102.8699
	1881.36
	115.1964
	1881.36
	160.1976
	1881.36
	123.9919
	1881.36
	125.3009
	1881.36
	119.4428

	1881.1
	19.77914
	1881.96
	-96.0753
	1881.97
	99.22064
	1881.97
	111.6967
	1881.97
	154.9293
	1881.97
	120.6528
	1881.97
	119.9254
	1881.97
	116.0145

	1881.72
	20.32074
	1882.58
	-96.6563
	1882.58
	95.91683
	1882.58
	108.7984
	1882.58
	149.2173
	1882.58
	117.9151
	1882.58
	114.1063
	1882.58
	112.9316

	1882.33
	20.86897
	1883.19
	-95.5979
	1883.2
	93.19607
	1883.2
	106.1774
	1883.2
	146.3789
	1883.2
	115.4575
	1883.2
	111.159
	1883.2
	110.4353

	1882.95
	21.4221
	1883.81
	-96.376
	1883.81
	91.40103
	1883.81
	103.1131
	1883.81
	141.2227
	1883.81
	112.5538
	1883.81
	105.8957
	1883.81
	108.8612

	1883.56
	21.97907
	1884.42
	-97.2183
	1884.43
	88.08203
	1884.43
	102.1461
	1884.43
	136.6247
	1884.43
	111.7501
	1884.43
	101.1888
	1884.43
	105.7667

	1884.18
	22.53802
	1885.03
	-97.4766
	1885.04
	85.39836
	1885.04
	99.39399
	1885.04
	131.9749
	1885.04
	109.1586
	1885.04
	96.43178
	1885.04
	103.3039

	1884.79
	23.09892
	1885.65
	-96.8476
	1885.65
	83.66404
	1885.65
	96.79017
	1885.65
	128.201
	1885.65
	106.7154
	1885.65
	92.5508
	1885.65
	101.7905

	1885.41
	23.66375
	1886.26
	-96.6994
	1886.27
	81.90178
	1886.27
	94.85862
	1886.27
	125.8468
	1886.27
	104.9471
	1886.27
	90.08767
	1886.27
	100.2527

	1886.02
	24.23491
	1886.87
	-97.065
	1886.88
	79.57276
	1886.88
	92.90323
	1886.88
	123.0322
	1886.88
	103.1524
	1886.88
	87.16592
	1886.88
	98.14458

	1886.63
	24.81458
	1887.49
	-96.8009
	1887.5
	77.36305
	1887.5
	90.03776
	1887.5
	120.368
	1887.5
	100.4502
	1887.5
	84.39279
	1887.5
	96.15938

	1887.25
	25.40279
	1888.1
	-96.6207
	1888.11
	74.52455
	1888.11
	89.13423
	1888.11
	117.2421
	1888.11
	99.70731
	1888.11
	81.1598
	1888.11
	93.54177

	1887.86
	25.99943
	1888.71
	-96.868
	1888.72
	71.61782
	1888.72
	86.32971
	1888.72
	112.6794
	1888.72
	97.06343
	1888.72
	76.48995
	1888.72
	90.85593

	1888.48
	26.60588
	1889.33
	-97.6966
	1889.34
	69.29604
	1889.34
	83.72538
	1889.34
	108.1029
	1889.34
	94.62238
	1889.34
	71.80455
	1889.34
	88.75865

	1889.09
	27.2239
	1889.94
	-98.4902
	1889.95
	68.19166
	1889.95
	82.00969
	1889.95
	104.1148
	1889.95
	93.06733
	1889.95
	67.70921
	1889.95
	87.87516

	1889.71
	27.85348
	1890.55
	-98.0888
	1890.56
	66.16271
	1890.56
	79.92211
	1890.56
	99.97963
	1890.56
	91.1404
	1890.56
	63.46695
	1890.56
	86.0671

	1890.32
	28.49556
	1891.16
	-97.2062
	1891.18
	65.09033
	1891.18
	77.98406
	1891.18
	97.67883
	1891.18
	89.36562
	1891.18
	61.05724
	1891.18
	85.21923

	1890.93
	29.15232
	1891.78
	-97.5945
	1891.79
	63.83976
	1891.79
	76.61461
	1891.79
	93.98523
	1891.79
	88.15682
	1891.79
	57.2565
	1891.79
	84.18954

	1891.55
	29.82496
	1892.39
	-98.5291
	1892.4
	61.73094
	1892.4
	74.94967
	1892.4
	91.37752
	1892.4
	86.65252
	1892.4
	54.54164
	1892.4
	82.30162

	1892.16
	30.51282
	1893
	-98.6452
	1893.02
	59.97616
	1893.02
	73.33758
	1893.02
	88.69509
	1893.02
	85.20371
	1893.02
	51.7503
	1893.02
	80.77134

	1892.77
	31.21761
	1893.62
	-98.2808
	1893.63
	58.49735
	1893.63
	72.02088
	1893.63
	85.61718
	1893.63
	84.04764
	1893.63
	48.56525
	1893.63
	79.51342

	1893.39
	31.94115
	1894.23
	-98.4626
	1894.24
	57.56461
	1894.24
	71.29633
	1894.24
	83.90574
	1894.24
	83.48373
	1894.24
	46.74666
	1894.24
	78.80157

	1894
	32.68366
	1894.84
	-98.7538
	1894.85
	56.85005
	1894.85
	70.425
	1894.85
	82.32856
	1894.85
	82.77304
	1894.85
	45.06233
	1894.85
	78.3079

	1894.61
	33.44628
	1895.45
	-99.5317
	1895.47
	54.67011
	1895.47
	68.93025
	1895.47
	81.11039
	1895.47
	81.44157
	1895.47
	43.73526
	1895.47
	76.35247

	1895.23
	34.22826
	1896.07
	-98.9764
	1896.08
	52.20255
	1896.08
	66.39979
	1896.08
	81.04257
	1896.08
	79.07175
	1896.08
	43.56029
	1896.08
	74.1058

	1895.84
	35.02818
	1896.68
	-99.7715
	1896.69
	51.54362
	1896.69
	64.95658
	1896.69
	80.27788
	1896.69
	77.78919
	1896.69
	42.68845
	1896.69
	73.66775

	1896.46
	35.84532
	1897.29
	-100.626
	1897.31
	50.61283
	1897.31
	63.40721
	1897.31
	81.0628
	1897.31
	76.40309
	1897.31
	43.36446
	1897.31
	72.96147

	1897.07
	36.67942
	1897.9
	-101.417
	1897.92
	49.9488
	1897.92
	60.74851
	1897.92
	80.97733
	1897.92
	73.90503
	1897.92
	43.17185
	1897.92
	72.51833

	1897.68
	37.53034
	1898.52
	-101.68
	1898.53
	48.95849
	1898.53
	60.64373
	1898.53
	79.00794
	1898.53
	73.9609
	1898.53
	41.09531
	1898.53
	71.74891

	1898.3
	38.39881
	1899.13
	-102.398
	1899.14
	47.00382
	1899.14
	58.98629
	1899.14
	74.99104
	1899.14
	72.4641
	1899.14
	36.97126
	1899.14
	70.01512

	1898.91
	39.28377
	1899.74
	-102.341
	1899.76
	45.35238
	1899.76
	55.95308
	1899.76
	72.16355
	1899.76
	69.59417
	1899.76
	34.03486
	1899.76
	68.5882

	1899.52
	40.18383
	1900.35
	-103.278
	1900.37
	43.41999
	1900.37
	53.67141
	1900.37
	68.78091
	1900.37
	67.47314
	1900.37
	30.54508
	1900.37
	66.8767

	1900.13
	41.09678
	1900.96
	-104.315
	1900.98
	41.92271
	1900.98
	51.17444
	1900.98
	67.49533
	1900.98
	65.13681
	1900.98
	29.15235
	1900.98
	65.6003

	1900.75
	42.02001
	1901.58
	-105.378
	1901.59
	39.7764
	1901.59
	49.0512
	1901.59
	65.53681
	1901.59
	63.17422
	1901.59
	27.08668
	1901.59
	63.67488

	1901.36
	42.95217
	1902.19
	-105.497
	1902.21
	38.99347
	1902.21
	45.89306
	1902.21
	62.22921
	1902.21
	60.17935
	1902.21
	23.67018
	1902.21
	63.11646

	1901.97
	43.89343
	1902.8
	-105.061
	1902.82
	38.01554
	1902.82
	43.38069
	1902.82
	59.44573
	1902.82
	57.82762
	1902.82
	20.77955
	1902.82
	62.35942

	1902.59
	44.84462
	1903.41
	-105.764
	1903.43
	36.41931
	1903.43
	41.53252
	1903.43
	55.75239
	1903.43
	56.14009
	1903.43
	16.97907
	1903.43
	60.98408

	1903.2
	45.80462
	1904.02
	-104.368
	1904.04
	34.30974
	1904.04
	39.4716
	1904.04
	52.51494
	1904.04
	54.23981
	1904.04
	13.63447
	1904.04
	59.0954

	1903.81
	46.77108
	1904.64
	-103.91
	1904.65
	33.13299
	1904.65
	37.34707
	1904.65
	50.17931
	1904.65
	52.27593
	1904.65
	11.19169
	1904.65
	58.13953

	1904.42
	47.74173
	1905.25
	-104.248
	1905.27
	31.83961
	1905.27
	34.60293
	1905.27
	48.92851
	1905.27
	49.69506
	1905.27
	9.83199
	1905.27
	57.07066

	1905.04
	48.71559
	1905.86
	-102.728
	1905.88
	30.51436
	1905.88
	32.47888
	1905.88
	47.98165
	1905.88
	47.73165
	1905.88
	8.77797
	1905.88
	55.9663

	1905.65
	49.6885
	1906.47
	-103.296
	1906.49
	29.23381
	1906.49
	31.26698
	1906.49
	46.81361
	1906.49
	46.68039
	1906.49
	7.50279
	1906.49
	54.90664

	1906.26
	50.65566
	1907.08
	-102.409
	1907.1
	27.38576
	1907.1
	29.82124
	1907.1
	44.94747
	1907.1
	45.3953
	1907.1
	5.5295
	1907.1
	53.27948

	1906.87
	51.61581
	1907.69
	-101.399
	1907.71
	25.66123
	1907.71
	28.31413
	1907.71
	43.36487
	1907.71
	44.04883
	1907.71
	3.83975
	1907.71
	51.77584

	1907.49
	52.56827
	1908.3
	-100.698
	1908.32
	24.30651
	1908.32
	26.21232
	1908.32
	40.20246
	1908.32
	42.10766
	1908.32
	0.57019
	1908.32
	50.64201

	1908.1
	53.51041
	1908.92
	-100.349
	1908.94
	21.77184
	1908.94
	23.85187
	1908.94
	37.60822
	1908.94
	39.91049
	1908.94
	-2.13295
	1908.94
	48.33184

	1908.71
	54.44071
	1909.53
	-100.904
	1909.55
	20.16921
	1909.55
	22.72916
	1909.55
	35.96282
	1909.55
	38.94842
	1909.55
	-3.8855
	1909.55
	46.95011

	1909.32
	55.35736
	1910.14
	-99.9174
	1910.16
	19.13561
	1910.16
	21.10233
	1910.16
	32.96408
	1910.16
	37.48223
	1910.16
	-6.99139
	1910.16
	46.13739

	1909.94
	56.25966
	1910.75
	-101.868
	1910.77
	17.99926
	1910.77
	20.62883
	1910.77
	31.09318
	1910.77
	37.16937
	1910.77
	-8.96943
	1910.77
	45.22193

	1910.55
	57.14665
	1911.36
	-101.992
	1911.38
	16.6552
	1911.38
	19.99835
	1911.38
	30.0091
	1911.38
	36.69954
	1911.38
	-10.1607
	1911.38
	44.09876

	1911.16
	58.0147
	1911.97
	-101.262
	1911.99
	15.66174
	1911.99
	18.58749
	1911.99
	30.14089
	1911.99
	35.44932
	1911.99
	-10.136
	1911.99
	43.32618

	1911.77
	58.86041
	1912.58
	-101.858
	1912.61
	14.86347
	1912.61
	17.39105
	1912.61
	28.87503
	1912.61
	34.41615
	1912.61
	-11.5108
	1912.61
	42.75243

	1912.38
	59.68281
	1913.19
	-101.639
	1913.22
	15.08936
	1913.22
	17.99203
	1913.22
	28.15697
	1913.22
	35.17777
	1913.22
	-12.336
	1913.22
	43.1992

	1913
	60.47971
	1913.8
	-101.736
	1913.83
	14.58249
	1913.83
	16.39732
	1913.83
	28.54753
	1913.83
	33.74371
	1913.83
	-12.0526
	1913.83
	42.91322

	1913.61
	61.24988
	1914.42
	-102.287
	1914.44
	13.82661
	1914.44
	16.56497
	1914.44
	28.70673
	1914.44
	34.072
	1914.44
	-12.0005
	1914.44
	42.37823

	1914.22
	61.99294
	1915.03
	-102.872
	1915.05
	12.27838
	1915.05
	16.46889
	1915.05
	27.43396
	1915.05
	34.13657
	1915.05
	-13.3805
	1915.05
	41.05089

	1914.83
	62.7082
	1915.64
	-103.406
	1915.66
	12.25185
	1915.66
	14.8229
	1915.66
	25.78466
	1915.66
	32.65121
	1915.66
	-15.1369
	1915.66
	41.24525

	1915.44
	63.39638
	1916.25
	-102.609
	1916.27
	11.84532
	1916.27
	14.1069
	1916.27
	25.934
	1916.27
	32.09586
	1916.27
	-15.0947
	1916.27
	41.05961

	1916.05
	64.05891
	1916.86
	-102.609
	1916.88
	10.47736
	1916.88
	12.91981
	1916.88
	25.05877
	1916.88
	31.06941
	1916.88
	-16.0771
	1916.88
	39.91253

	1916.66
	64.69677
	1917.47
	-101.34
	1917.49
	10.29195
	1917.49
	11.81782
	1917.49
	23.10628
	1917.49
	30.12806
	1917.49
	-18.1367
	1917.49
	39.94801

	1917.28
	65.3122
	1918.08
	-102.263
	1918.1
	10.56648
	1918.1
	10.68454
	1918.1
	21.23354
	1918.1
	29.15542
	1918.1
	-20.1166
	1918.1
	40.44343

	1917.89
	65.90527
	1918.69
	-101.821
	1918.71
	9.33768
	1918.71
	10.02126
	1918.71
	19.75434
	1918.71
	28.65279
	1918.71
	-21.703
	1918.71
	39.43551

	1918.5
	66.47704
	1919.3
	-101.732
	1919.32
	9.22671
	1919.32
	7.97896
	1919.32
	17.91788
	1919.32
	26.77113
	1919.32
	-23.6466
	1919.32
	39.54544

	1919.11
	67.0302
	1919.91
	-102.005
	1919.94
	8.87899
	1919.94
	8.00912
	1919.94
	16.46729
	1919.94
	26.96457
	1919.94
	-25.2061
	1919.94
	39.42223

	1919.72
	67.5646
	1920.52
	-102.298
	1920.55
	8.58019
	1920.55
	6.8482
	1920.55
	15.62259
	1920.55
	25.96428
	1920.55
	-26.1579
	1920.55
	39.34431

	1920.33
	68.07923
	1921.13
	-101.831
	1921.16
	7.03544
	1921.16
	5.48892
	1921.16
	14.59627
	1921.16
	24.76565
	1921.16
	-27.2914
	1921.16
	38.02045

	1920.94
	68.57535
	1921.74
	-101.889
	1921.77
	6.94834
	1921.77
	6.01945
	1921.77
	12.57642
	1921.77
	25.45681
	1921.77
	-29.4184
	1921.77
	38.15424

	1921.55
	69.04963
	1922.35
	-101.526
	1922.38
	5.83046
	1922.38
	5.03527
	1922.38
	10.99461
	1922.38
	24.63328
	1922.38
	-31.1073
	1922.38
	37.25724

	1922.17
	69.49675
	1922.96
	-101.986
	1922.99
	3.39983
	1922.99
	4.31521
	1922.99
	10.43496
	1922.99
	24.07386
	1922.99
	-31.7741
	1922.99
	35.0475

	1922.78
	69.91503
	1923.57
	-101.859
	1923.6
	2.34469
	1923.6
	4.40103
	1923.6
	9.11687
	1923.6
	24.32032
	1923.6
	-33.1994
	1923.6
	34.21325

	1923.39
	70.30565
	1924.18
	-102.426
	1924.21
	2.27714
	1924.21
	3.37105
	1924.21
	8.76442
	1924.21
	23.45098
	1924.21
	-33.659
	1924.21
	34.36659

	1924
	70.66644
	1924.79
	-100.786
	1924.82
	2.09502
	1924.82
	1.77645
	1924.82
	7.23466
	1924.82
	22.01702
	1924.82
	-35.2959
	1924.82
	34.40536

	1924.61
	70.99747
	1925.4
	-100.593
	1925.43
	1.91133
	1925.43
	1.05635
	1925.43
	4.93921
	1925.43
	21.45757
	1925.43
	-37.6985
	1925.43
	34.44255

	1925.22
	71.29923
	1926.01
	-101.108
	1926.04
	0.6443
	1926.04
	-0.21139
	1926.04
	3.2669
	1926.04
	20.35048
	1926.04
	-39.4779
	1926.04
	33.39642

	1925.83
	71.57095
	1926.62
	-99.7397
	1926.65
	0.72865
	1926.65
	0.1997
	1926.65
	2.55596
	1926.65
	20.9222
	1926.65
	-40.296
	1926.65
	33.70166

	1926.44
	71.81097
	1927.23
	-99.0661
	1927.26
	1.0079
	1927.26
	0.02262
	1927.26
	1.41659
	1927.26
	20.84452
	1927.26
	-41.5425
	1927.26
	34.2018

	1927.05
	72.01906
	1927.84
	-99.0424
	1927.87
	0.532
	1927.87
	0.45045
	1927.87
	0.13383
	1927.87
	21.05515
	1927.87
	-42.9324
	1927.87
	33.94678

	1927.66
	72.19399
	1928.45
	-98.8148
	1928.48
	-0.09554
	1928.48
	1.217
	1928.48
	-0.25348
	1928.48
	21.60449
	1928.48
	-43.425
	1928.48
	33.54013

	1928.27
	72.33307
	1929.06
	-99.4879
	1929.09
	-0.47974
	1929.09
	2.48355
	1929.09
	-1.07613
	1929.09
	22.65383
	1929.09
	-44.3518
	1929.09
	33.37682

	1928.88
	72.43466
	1929.67
	-99.4176
	1929.7
	-0.84061
	1929.7
	2.0252
	1929.7
	0.44298
	1929.7
	21.97827
	1929.7
	-42.9368
	1929.7
	33.23684

	1929.49
	72.49753
	1930.27
	-99.7119
	1930.31
	-1.07579
	1930.31
	2.93861
	1930.31
	3.40601
	1930.31
	22.67448
	1930.31
	-40.078
	1930.31
	33.22254

	1930.1
	72.5194
	1930.88
	-100.287
	1930.92
	-1.37038
	1930.92
	4.40928
	1930.92
	4.84689
	1930.92
	23.92794
	1930.92
	-38.7413
	1930.92
	33.14884

	1930.71
	72.49247
	1931.49
	-100.968
	1931.53
	-0.31307
	1931.53
	5.34572
	1931.53
	6.12124
	1931.53
	24.64717
	1931.53
	-37.5711
	1931.53
	34.42703

	1931.32
	72.41681
	1932.1
	-102.134
	1932.13
	0.71011
	1932.13
	6.27487
	1932.13
	8.15408
	1932.13
	25.36267
	1932.13
	-35.6407
	1932.13
	35.44464

	1931.93
	72.29544
	1932.71
	-102.411
	1932.74
	2.48308
	1932.74
	7.2615
	1932.74
	9.5947
	1932.74
	26.1321
	1932.74
	-34.3043
	1932.74
	37.06637

	1932.54
	72.13211
	1933.32
	-102.608
	1933.35
	3.86821
	1933.35
	8.47676
	1933.35
	11.8416
	1933.35
	27.13015
	1933.35
	-32.1615
	1933.35
	38.30025

	1933.15
	71.93451
	1933.93
	-103.631
	1933.96
	4.88314
	1933.96
	8.9128
	1933.96
	14.78654
	1933.96
	27.34898
	1933.96
	-29.3208
	1933.96
	39.16393

	1933.76
	71.70448
	1934.54
	-103.849
	1934.57
	5.91644
	1934.57
	10.54618
	1934.57
	15.22633
	1934.57
	28.76516
	1934.57
	-28.9851
	1934.57
	40.04599

	1934.37
	71.44529
	1935.15
	-103.92
	1935.18
	7.00013
	1935.18
	11.23054
	1935.18
	17.73592
	1935.18
	29.23231
	1935.18
	-26.5797
	1935.18
	40.97844

	1934.98
	71.16443
	1935.76
	-104.628
	1935.79
	8.27612
	1935.79
	12.17126
	1935.79
	20.36761
	1935.79
	29.95582
	1935.79
	-24.0522
	1935.79
	42.10318

	1935.59
	70.86241
	1936.36
	-105.062
	1936.4
	9.39759
	1936.4
	14.90629
	1936.4
	22.07009
	1936.4
	32.47365
	1936.4
	-22.4539
	1936.4
	43.07342

	1936.2
	70.54093
	1936.97
	-104.465
	1937.01
	10.09058
	1937.01
	16.83553
	1937.01
	24.32565
	1937.01
	34.18567
	1937.01
	-20.3025
	1937.01
	43.61516

	1936.81
	70.20429
	1937.58
	-104.564
	1937.62
	11.37258
	1937.62
	18.22182
	1937.62
	27.27866
	1937.62
	35.35476
	1937.62
	-17.4537
	1937.62
	44.74592

	1937.42
	69.85439
	1938.19
	-105.515
	1938.23
	13.36302
	1938.23
	19.15125
	1938.23
	31.03285
	1938.23
	36.06698
	1938.23
	-13.8036
	1938.23
	46.58511

	1938.03
	69.49098
	1938.8
	-104.412
	1938.84
	15.48536
	1938.84
	21.8984
	1938.84
	33.72188
	1938.84
	38.59693
	1938.84
	-11.2188
	1938.84
	48.55621

	1938.64
	69.11517
	1939.41
	-103.706
	1939.44
	17.77502
	1939.44
	24.67416
	1939.44
	37.36117
	1939.44
	41.15904
	1939.44
	-7.68194
	1939.44
	50.69711

	1939.25
	68.72971
	1940.02
	-104.5
	1940.05
	19.15932
	1940.05
	27.30955
	1940.05
	40.40491
	1940.05
	43.57722
	1940.05
	-4.74237
	1940.05
	51.93016

	1939.86
	68.33293
	1940.62
	-104.169
	1940.66
	21.5046
	1940.66
	28.60769
	1940.66
	43.39002
	1940.66
	44.65815
	1940.66
	-1.86143
	1940.66
	54.1242

	1940.47
	67.92786
	1941.23
	-103.535
	1941.27
	23.58178
	1941.27
	31.23081
	1941.27
	47.38018
	1941.27
	47.06407
	1941.27
	2.02456
	1941.27
	56.05013

	1941.08
	67.51943
	1941.84
	-104.055
	1941.88
	25.04582
	1941.88
	32.48315
	1941.88
	49.72465
	1941.88
	48.0992
	1941.88
	4.26486
	1941.88
	57.36293

	1941.68
	67.11111
	1942.45
	-103.623
	1942.49
	27.37319
	1942.49
	34.25765
	1942.49
	53.20069
	1942.49
	49.65649
	1942.49
	7.63673
	1942.49
	59.53906

	1942.29
	66.70406
	1943.06
	-103.87
	1943.09
	29.7647
	1943.09
	36.62259
	1943.09
	55.44085
	1943.09
	51.80778
	1943.09
	9.77443
	1943.09
	61.7818

	1942.9
	66.30272
	1943.66
	-103.978
	1943.7
	31.88025
	1943.7
	39.20148
	1943.7
	59.46566
	1943.7
	54.16947
	1943.7
	13.69507
	1943.7
	63.74611

	1943.51
	65.91131
	1944.27
	-103.426
	1944.31
	34.1207
	1944.31
	40.62704
	1944.31
	63.52105
	1944.31
	55.37782
	1944.31
	17.64629
	1944.31
	65.83532

	1944.12
	65.53197
	1944.88
	-103.062
	1944.92
	35.99658
	1944.92
	43.60915
	1944.92
	65.86855
	1944.92
	58.14272
	1944.92
	19.88962
	1944.92
	67.55996

	1944.73
	65.16838
	1945.49
	-103.63
	1945.53
	36.86933
	1945.53
	44.14067
	1945.53
	68.14409
	1945.53
	58.45704
	1945.53
	22.06099
	1945.53
	68.28146

	1945.34
	64.82232
	1946.1
	-103.487
	1946.14
	39.50776
	1946.14
	47.01651
	1946.14
	73.07727
	1946.14
	61.11567
	1946.14
	26.89
	1946.14
	70.76865

	1945.95
	64.49364
	1946.7
	-102.766
	1946.74
	41.51234
	1946.74
	50.57702
	1946.74
	77.40836
	1946.74
	64.46253
	1946.74
	31.11863
	1946.74
	72.62447

	1946.55
	64.17819
	1947.31
	-103.07
	1947.35
	44.21836
	1947.35
	53.12804
	1947.35
	80.83384
	1947.35
	66.79634
	1947.35
	34.43994
	1947.35
	75.17925

	1947.16
	63.87512
	1947.92
	-104.23
	1947.96
	46.34935
	1947.96
	55.06231
	1947.96
	84.79114
	1947.96
	68.5134
	1947.96
	38.29307
	1947.96
	77.15898

	1947.77
	63.58364
	1948.53
	-104.512
	1948.57
	47.06831
	1948.57
	55.77999
	1948.57
	88.01898
	1948.57
	69.01388
	1948.57
	41.41674
	1948.57
	77.7267

	1948.38
	63.30233
	1949.13
	-104.568
	1949.18
	48.07413
	1949.18
	58.19081
	1949.18
	93.2974
	1949.18
	71.2075
	1949.18
	46.591
	1949.18
	78.58128

	1948.99
	63.03704
	1949.74
	-104.203
	1949.78
	50.7114
	1949.78
	61.51611
	1949.78
	98.14608
	1949.78
	74.31915
	1949.78
	51.33721
	1949.78
	81.06978

	1949.6
	62.78985
	1950.35
	-104.14
	1950.39
	52.48442
	1950.39
	64.02447
	1950.39
	102.6231
	1950.39
	76.6103
	1950.39
	55.71004
	1950.39
	82.69156

	1950.2
	62.56267
	1950.96
	-103.473
	1951
	54.29018
	1951
	65.35478
	1951
	106.7232
	1951
	77.72341
	1951
	59.706
	1951
	84.34608

	1950.81
	62.35888
	1951.56
	-103.006
	1951.61
	57.75928
	1951.61
	67.57765
	1951.61
	111.6281
	1951.61
	79.72906
	1951.61
	64.50667
	1951.61
	87.66393

	1951.42
	62.17662
	1952.17
	-103.033
	1952.21
	59.97231
	1952.21
	68.79586
	1952.21
	116.4627
	1952.21
	80.73363
	1952.21
	69.23886
	1952.21
	89.7282

	1952.03
	62.01244
	1952.78
	-102.644
	1952.82
	61.59409
	1952.82
	69.71782
	1952.82
	120.5038
	1952.82
	81.43839
	1952.82
	73.17575
	1952.82
	91.19874

	1952.64
	61.86152
	1953.38
	-102.046
	1953.43
	62.73836
	1953.43
	70.55929
	1953.43
	124.1016
	1953.43
	82.06264
	1953.43
	76.66945
	1953.43
	92.19177

	1953.25
	61.72206
	1953.99
	-101.046
	1954.03
	65.64329
	1954.03
	72.12287
	1954.03
	127.5647
	1954.03
	83.41258
	1954.03
	80.03001
	1954.03
	94.94793

	1953.85
	61.59146
	1954.6
	-100.808
	1954.64
	67.78952
	1954.64
	73.35022
	1954.64
	132.4088
	1954.64
	84.42272
	1954.64
	84.76999
	1954.64
	96.94292

	1954.46
	61.46582
	1955.21
	-99.9548
	1955.25
	68.84988
	1955.25
	75.74187
	1955.25
	135.4233
	1955.25
	86.59717
	1955.25
	87.68035
	1955.25
	97.85203

	1955.07
	61.34048
	1955.81
	-99.0336
	1955.86
	71.03023
	1955.86
	77.52196
	1955.86
	139.7253
	1955.86
	88.16005
	1955.86
	91.87817
	1955.86
	99.88114

	1955.68
	61.20618
	1956.42
	-98.9743
	1956.46
	71.51529
	1956.46
	78.60916
	1956.46
	144.4444
	1956.46
	89.0336
	1956.46
	96.49475
	1956.46
	100.2174

	1956.29
	61.05608
	1957.02
	-98.8536
	1957.07
	72.64774
	1957.07
	80.19776
	1957.07
	147.6347
	1957.07
	90.405
	1957.07
	99.58095
	1957.07
	101.1986

	1956.89
	60.88622
	1957.63
	-100.153
	1957.68
	73.65719
	1957.68
	81.66076
	1957.68
	151.0927
	1957.68
	91.65079
	1957.68
	102.9347
	1957.68
	102.0569

	1957.5
	60.69128
	1958.24
	-100.43
	1958.28
	73.25984
	1958.28
	82.88255
	1958.28
	154.7048
	1958.28
	92.65893
	1958.28
	106.4444
	1958.28
	101.5107

	1958.11
	60.46236
	1958.85
	-101.523
	1958.89
	73.95719
	1958.89
	84.87253
	1958.89
	156.2981
	1958.89
	94.4317
	1958.89
	107.9335
	1958.89
	102.0568

	1958.72
	60.19052
	1959.45
	-101.72
	1959.5
	75.06762
	1959.5
	86.12964
	1959.5
	157.9608
	1959.5
	95.47161
	1959.5
	109.492
	1959.5
	103.016

	1959.32
	59.86942
	1960.06
	-102.132
	1960.1
	74.98694
	1960.1
	87.0332
	1960.1
	157.7061
	1960.1
	96.16152
	1960.1
	109.1348
	1960.1
	102.7866

	1959.93
	59.49404
	1960.66
	-103.581
	1960.71
	75.29613
	1960.71
	88.16334
	1960.71
	158.8757
	1960.71
	97.07445
	1960.71
	110.2003
	1960.71
	102.9445

	1960.54
	59.06082
	1961.27
	-103.629
	1961.32
	77.22257
	1961.32
	88.00034
	1961.32
	159.085
	1961.32
	96.69425
	1961.32
	110.3054
	1961.32
	104.7197

	1961.14
	58.56875
	1961.88
	-103.765
	1961.93
	78.33092
	1961.93
	88.47527
	1961.93
	160.4493
	1961.93
	96.95197
	1961.93
	111.5656
	1961.93
	105.6768

	1961.75
	58.01845
	1962.48
	-103.896
	1962.53
	77.87999
	1962.53
	88.67675
	1962.53
	160.2635
	1962.53
	96.9398
	1962.53
	111.2774
	1962.53
	105.0771

	1962.36
	57.40677
	1963.09
	-104.044
	1963.14
	77.88539
	1963.14
	89.28482
	1963.14
	159.8579
	1963.14
	97.33066
	1963.14
	110.7675
	1963.14
	104.9313

	1962.97
	56.73008
	1963.7
	-104.898
	1963.74
	78.27969
	1963.74
	89.75972
	1963.74
	160.563
	1963.74
	97.59191
	1963.74
	111.3702
	1963.74
	105.1768

	1963.57
	55.98931
	1964.3
	-105.084
	1964.35
	77.43112
	1964.35
	89.88335
	1964.35
	159.4055
	1964.35
	97.49834
	1964.35
	110.1085
	1964.35
	104.177

	1964.18
	55.18205
	1964.91
	-104.593
	1964.96
	76.5794
	1964.96
	90.14033
	1964.96
	158.7702
	1964.96
	97.53811
	1964.96
	109.369
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	103.1741

	1964.79
	54.31591
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	-102.78
	1965.56
	76.76247
	1965.56
	90.31786
	1965.56
	160.6421
	1965.56
	97.50199
	1965.56
	111.1385
	1965.56
	103.2084

	1965.39
	53.39758
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	-102.477
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	75.3635
	1966.17
	90.73012
	1966.17
	159.0095
	1966.17
	97.69705
	1966.17
	109.4018
	1966.17
	101.6582
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	52.43535
	1966.72
	-102.937
	1966.78
	73.29212
	1966.78
	90.62169
	1966.78
	157.9863
	1966.78
	97.3714
	1966.78
	108.2743
	1966.78
	99.43552

	1966.61
	51.43779
	1967.33
	-102.651
	1967.38
	72.1859
	1967.38
	89.62714
	1967.38
	155.8351
	1967.38
	96.16321
	1967.38
	106.0207
	1967.38
	98.18055

	1967.21
	50.41558
	1967.94
	-102.123
	1967.99
	72.43707
	1967.99
	88.39851
	1967.99
	153.4089
	1967.99
	94.71737
	1967.99
	103.4903
	1967.99
	98.28047

	1967.82
	49.38137
	1968.54
	-101.939
	1968.59
	71.25394
	1968.59
	86.00071
	1968.59
	151.3464
	1968.59
	92.10593
	1968.59
	101.3254
	1968.59
	96.94857

	1968.43
	48.34131
	1969.15
	-101.827
	1969.2
	70.54446
	1969.2
	86.02765
	1969.2
	150.4688
	1969.2
	91.91566
	1969.2
	100.3436
	1969.2
	96.08785

	1969.03
	47.3053
	1969.75
	-101.816
	1969.81
	69.52341
	1969.81
	84.23851
	1969.81
	147.9961
	1969.81
	89.90932
	1969.81
	97.76672
	1969.81
	94.91556

	1969.64
	46.28472
	1970.36
	-100.98
	1970.41
	68.72871
	1970.41
	82.0417
	1970.41
	146.1711
	1970.41
	87.49886
	1970.41
	95.83925
	1970.41
	93.97209

	1970.25
	45.28658
	1970.96
	-99.8931
	1971.02
	70.17544
	1971.02
	81.4548
	1971.02
	145.2266
	1971.02
	86.69475
	1971.02
	94.79056
	1971.02
	95.26758

	1970.85
	44.31605
	1971.57
	-99.8891
	1971.62
	69.81617
	1971.62
	79.86611
	1971.62
	142.8817
	1971.62
	84.89241
	1971.62
	92.34323
	1971.62
	94.75955

	1971.46
	43.3717
	1972.17
	-100.719
	1972.23
	69.67859
	1972.23
	76.86313
	1972.23
	140.0272
	1972.23
	81.67223
	1972.23
	89.38453
	1972.23
	94.47073

	1972.07
	42.45092
	1972.78
	-101.258
	1972.83
	68.73926
	1972.83
	76.5053
	1972.83
	138.7405
	1972.83
	81.10075
	1972.83
	87.99539
	1972.83
	93.38263

	1972.67
	41.55809
	1973.38
	-101.597
	1973.44
	66.43593
	1973.44
	74.69084
	1973.44
	136.2642
	1973.44
	79.06908
	1973.44
	85.41487
	1973.44
	90.92806

	1973.28
	40.69936
	1973.99
	-101.137
	1974.05
	64.68026
	1974.05
	72.54853
	1974.05
	134.437
	1974.05
	76.70957
	1974.05
	83.48357
	1974.05
	89.02114

	1973.88
	39.87071
	1974.6
	-100.775
	1974.65
	63.40504
	1974.65
	70.42208
	1974.65
	131.7737
	1974.65
	74.36947
	1974.65
	80.71776
	1974.65
	87.59716

	1974.49
	39.06846
	1975.2
	-101.666
	1975.26
	61.43911
	1975.26
	68.63593
	1975.26
	129.2065
	1975.26
	72.36611
	1975.26
	78.0464
	1975.26
	85.47998

	1975.1
	38.29129
	1975.81
	-101.394
	1975.86
	59.2807
	1975.86
	67.60231
	1975.86
	127.7966
	1975.86
	71.11884
	1975.86
	76.53407
	1975.86
	83.17281

	1975.7
	37.53732
	1976.41
	-101.484
	1976.47
	59.24672
	1976.47
	67.0544
	1976.47
	124.5888
	1976.47
	70.35372
	1976.47
	73.22212
	1976.47
	82.98759

	1976.31
	36.80673
	1977.02
	-102
	1977.07
	57.97021
	1977.07
	64.93614
	1977.07
	120.0711
	1977.07
	68.02183
	1977.07
	68.60189
	1977.07
	81.56232

	1976.91
	36.10192
	1977.62
	-101.034
	1977.68
	56.13638
	1977.68
	62.26616
	1977.68
	117.2554
	1977.68
	65.13463
	1977.68
	65.68205
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	79.57724

	1977.52
	35.42158
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	-100.198
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	55.37732
	1978.28
	60.40262
	1978.28
	113.4251
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	63.05744
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	61.74926
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	78.66941
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	34.7544
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	-101.329
	1978.89
	53.7993
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	58.72624
	1978.89
	109.0256
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	61.16386
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	57.24564
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	76.94016

	1978.73
	34.09064
	1979.43
	-101.173
	1979.49
	52.47573
	1979.49
	58.06466
	1979.49
	107.7375
	1979.49
	60.28863
	1979.49
	55.85502
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	75.46782

	1979.34
	33.42477
	1980.04
	-101.063
	1980.1
	51.47027
	1980.1
	56.1477
	1980.1
	103.3759
	1980.1
	58.15447
	1980.1
	51.38924
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	74.31111

	1979.94
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	1980.64
	-100.613
	1980.7
	49.27305
	1980.7
	53.5051
	1980.7
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	1980.7
	55.29822
	1980.7
	47.75635
	1980.7
	71.96513
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	-102.129
	1981.31
	47.88955
	1981.31
	52.05657
	1981.31
	97.3097
	1981.31
	53.63249
	1981.31
	45.11645
	1981.31
	70.43038

	1981.15
	31.39408
	1981.85
	-101.336
	1981.91
	47.47076
	1981.91
	50.06496
	1981.91
	93.70731
	1981.91
	51.42723
	1981.91
	41.4116
	1981.91
	69.86283

	1981.76
	30.71277
	1982.46
	-102.417
	1982.52
	44.90459
	1982.52
	48.79091
	1982.52
	92.07187
	1982.52
	49.93597
	1982.52
	39.67199
	1982.52
	67.14542

	1982.36
	30.02626
	1983.06
	-102.844
	1983.12
	42.85972
	1983.12
	47.80812
	1983.12
	88.37693
	1983.12
	48.73953
	1983.12
	35.87458
	1983.12
	64.95179

	1982.97
	29.32979
	1983.66
	-103.221
	1983.72
	41.26872
	1983.72
	46.52188
	1983.72
	85.51703
	1983.72
	47.23965
	1983.72
	32.91223
	1983.72
	63.21202

	1983.57
	28.63177
	1984.27
	-104.19
	1984.33
	38.82039
	1984.33
	45.01979
	1984.33
	81.28061
	1984.33
	45.52035
	1984.33
	28.57163
	1984.33
	60.61245

	1984.18
	27.93463
	1984.87
	-105.81
	1984.93
	35.48023
	1984.93
	41.73598
	1984.93
	74.87657
	1984.93
	42.0229
	1984.93
	22.06513
	1984.93
	57.12353

	1984.78
	27.24164
	1985.48
	-103.975
	1985.54
	32.69195
	1985.54
	38.74802
	1985.54
	69.25742
	1985.54
	38.81773
	1985.54
	16.34182
	1985.54
	54.18401

	1985.39
	26.55994
	1986.08
	-104.435
	1986.14
	29.79874
	1986.14
	36.70816
	1986.14
	63.34985
	1986.14
	36.56422
	1986.14
	10.33178
	1986.14
	51.14203

	1985.99
	25.89334
	1986.68
	-104.204
	1986.75
	27.60923
	1986.75
	32.96973
	1986.75
	58.15081
	1986.75
	32.60858
	1986.75
	5.02857
	1986.75
	48.80128

	1986.6
	25.23387
	1987.29
	-104.718
	1987.35
	26.50903
	1987.35
	29.65216
	1987.35
	52.17708
	1987.35
	29.07736
	1987.35
	-1.04762
	1987.35
	47.55231

	1987.2
	24.55935
	1987.89
	-104.747
	1987.95
	23.64387
	1987.95
	26.62101
	1987.95
	47.88316
	1987.95
	25.83257
	1987.95
	-5.444
	1987.95
	44.53839

	1987.81
	23.84006
	1988.5
	-104.896
	1988.56
	20.36599
	1988.56
	24.3552
	1988.56
	42.87485
	1988.56
	23.34956
	1988.56
	-10.5565
	1988.56
	41.10926

	1988.41
	23.05457
	1989.1
	-104.746
	1989.16
	18.29363
	1989.16
	21.84925
	1989.16
	38.71449
	1989.16
	20.62995
	1989.16
	-14.8193
	1989.16
	38.88815

	1989.02
	22.20553
	1989.7
	-105.126
	1989.77
	15.90343
	1989.77
	18.94314
	1989.77
	35.45429
	1989.77
	17.50664
	1989.77
	-18.1837
	1989.77
	36.34669

	1989.62
	21.28535
	1990.31
	-105.011
	1990.37
	14.77944
	1990.37
	17.48848
	1990.37
	32.91481
	1990.37
	15.83833
	1990.37
	-20.8256
	1990.37
	35.07394

	1990.23
	20.28494
	1990.91
	-104.956
	1990.97
	14.04744
	1990.97
	13.69334
	1990.97
	28.62627
	1990.97
	11.82954
	1990.97
	-25.2166
	1990.97
	34.19318

	1990.83
	19.19303
	1991.51
	-105.55
	1991.58
	14.98998
	1991.58
	10.64704
	1991.58
	27.60543
	1991.58
	8.56604
	1991.58
	-26.3416
	1991.58
	34.98448

	1991.43
	18.00529
	1992.12
	-107.014
	1992.18
	14.41008
	1992.18
	10.55941
	1992.18
	26.0388
	1992.18
	8.26476
	1992.18
	-28.0107
	1992.18
	34.25581

	1992.04
	16.72056
	1992.72
	-108.815
	1992.79
	12.52218
	1992.79
	8.16707
	1992.79
	22.85992
	1992.79
	5.65522
	1992.79
	-31.2938
	1992.79
	32.21667

	1992.64
	15.35012
	1993.32
	-109.149
	1993.39
	8.00817
	1993.39
	8.10162
	1993.39
	18.46433
	1993.39
	5.37612
	1993.39
	-35.7918
	1993.39
	27.55389

	1993.25
	13.89374
	1993.93
	-109.321
	1993.99
	3.55185
	1993.99
	9.44388
	1993.99
	16.55566
	1993.99
	6.50473
	1993.99
	-37.803
	1993.99
	22.94881

	1993.85
	12.27921
	1994.53
	-108.772
	1994.6
	3.7883
	1994.6
	6.84911
	1994.6
	11.1953
	1994.6
	3.69275
	1994.6
	-43.2675
	1994.6
	23.03402

	1994.46
	10.35459
	1995.13
	-108.449
	1995.2
	2.95543
	1995.2
	5.32139
	1995.2
	7.34496
	1995.2
	1.95139
	1995.2
	-47.2203
	1995.2
	22.05238

	1995.06
	8.19087
	1995.74
	-108.628
	1995.8
	5.83184
	1995.8
	4.96759
	1995.8
	5.31654
	1995.8
	1.38394
	1995.8
	-49.3512
	1995.8
	24.78003

	1995.66
	5.76487
	1996.34
	-108.58
	1996.41
	4.80868
	1996.41
	0.97263
	1996.41
	7.5778
	1996.41
	-2.82823
	1996.41
	-47.1941
	1996.41
	23.60563

	1996.27
	2.91393
	1996.94
	-109.248
	1997.01
	0.79261
	1997.01
	-0.26865
	1997.01
	5.56061
	1997.01
	-4.28315
	1997.01
	-49.3137
	1997.01
	19.44079

	1996.87
	-0.66532
	1997.54
	-109.601
	1997.61
	1.36503
	1997.61
	0.20946
	1997.61
	7.6447
	1997.61
	-4.01869
	1997.61
	-47.3321
	1997.61
	19.86445

	1997.47
	-4.85316
	1998.15
	-107.611
	1998.22
	0
	1998.22
	######
	1998.22
	0
	1998.22
	-4.44536
	1998.22
	-55.081
	1998.22
	18.34817

	1998.08
	-8.65377
	1998.75
	-108.395
	1998.82
	-18.046
	1998.82
	-4.35468
	1998.82
	-10.522
	1998.82
	-9.01368
	1998.82
	-65.7055
	1998.82
	0.15344

	1998.68
	-13.5544
	1999.35
	-111.372
	1999.42
	-30.753
	1999.42
	-18.7857
	1999.42
	-71.4867
	1999.42
	-23.6584
	1999.42
	-126.773
	1999.42
	-12.7023

	1999.29
	-21.9084
	1999.96
	-113.807
	1999.45
	-62.5585
	1999.45
	-64.2143
	1999.45
	-151.167
	1999.45
	-69.0976
	1999.45
	-206.458
	1999.45
	-44.5153




Table S6. Eccentricity statistics of different groups of NPs.
	Commercialized NPs
	Self-made NPs
	Naturally-derived NPs

	
	Area
	Angle
	Size (length)
	Size (width)
	Eccentricity
	
	Area
	Angle
	Size (length)
	Size (width)
	Eccentricity
	
	Area
	Angle
	Size (length)
	Size (width)
	Eccentricity

	1
	128.4269
	65.2738
	33.45203
	1.951266
	0.737356
	1
	51.12323
	211.8909
	180.4325
	1.17435
	0.274888
	1
	83.92727
	217.3941
	186.4578
	1.165916
	0.26436

	2
	27.60772
	74.32281
	26.30844
	2.825056
	0.874701
	2
	9.49547
	84.10376
	57.80521
	1.454951
	0.527607
	2
	130.3198
	186.1384
	186.061
	1.000416
	0.000831

	3
	120.8743
	59.16776
	25.69424
	2.302764
	0.811418
	3
	76.8485
	55.00751
	48.01135
	1.145719
	0.238195
	3
	102.8392
	200.769
	160.6791
	1.249503
	0.359491

	4
	90
	37
	35
	1.057143
	0.105186
	4
	127.0528
	67.97177
	47.68233
	1.425513
	0.507895
	4
	122.2697
	174.5122
	117.2835
	1.487952
	0.548329

	5
	180
	35.00006
	35
	1.000002
	3.43E-06
	5
	117.2407
	60.17126
	32.23199
	1.866818
	0.713057
	5
	160.3207
	135.4504
	82.51981
	1.641429
	0.628845

	6
	180
	35
	35
	1
	0
	6
	179.2176
	65.34293
	30.57831
	2.136905
	0.781007
	6
	52.42703
	103.4639
	86.50756
	1.19601
	0.300914

	7
	180
	35
	35
	1
	0
	7
	125.4936
	63.25586
	29.54495
	2.141004
	0.781845
	7
	178.9376
	126.958
	76.95386
	1.649794
	0.632599

	8
	180
	35
	35
	1
	0
	8
	133.7276
	47.81686
	39.33096
	1.215756
	0.323439
	8
	78.62955
	100.0857
	69.9523
	1.430771
	0.511505

	9
	90
	35
	35
	1
	0
	9
	176.3997
	54.09052
	31.90146
	1.69555
	0.652161
	9
	160.9083
	87.78128
	69.75525
	1.258418
	0.368534

	10
	90
	35
	33
	1.060606
	0.11102
	10
	74.6982
	43.3587
	33.94877
	1.27718
	0.38695
	10
	15.91475
	116.4319
	66.86866
	1.741203
	0.670162

	11
	132.614
	33.41129
	32.85195
	1.017026
	0.033202
	11
	4.04107
	55.36055
	28.27698
	1.957796
	0.739105
	11
	23.30879
	106.4246
	47.04959
	2.261967
	0.804554

	12
	90
	33
	33
	1
	0
	12
	117.6666
	53.39777
	27.70023
	1.927701
	0.730896
	12
	102.8152
	94.65283
	68.75485
	1.376671
	0.472358

	13
	90
	33
	33
	1
	0
	13
	101.2473
	44.72424
	39.46472
	1.133271
	0.221368
	13
	153.4441
	81.53949
	68.06934
	1.197889
	0.303105

	14
	90
	33
	33
	1
	0
	14
	66.29077
	46.22705
	34.49014
	1.340298
	0.44333
	14
	29.59531
	74.56863
	64.021
	1.164753
	0.26289

	15
	1.82661
	33.20636
	31.20737
	1.064055
	0.116774
	15
	129.0647
	61.29134
	22.61447
	2.710271
	0.863863
	15
	71.86674
	74.22833
	60.15659
	1.233919
	0.343209

	16
	90
	33
	31
	1.064516
	0.117539
	16
	61.56537
	47.65765
	31.7811
	1.499559
	0.555294
	16
	149.6993
	68.63689
	61.77428
	1.111092
	0.189972

	17
	180
	31
	31
	1
	0
	17
	27.19413
	55.65302
	26.50879
	2.099418
	0.773117
	17
	7.31762
	88.64755
	74.69009
	1.186872
	0.290108

	18
	27.82318
	42.57324
	21.54422
	1.976086
	0.743913
	18
	29.12935
	54.22849
	28.71759
	1.888337
	0.719559
	18
	145.0721
	68.81534
	57.40659
	1.198736
	0.30409

	19
	0.56423
	31.06743
	29.06752
	1.068802
	0.124602
	19
	13.64577
	55.28436
	29.31073
	1.886147
	0.718908
	19
	43.92063
	64.85364
	50.79453
	1.276784
	0.38657

	20
	0.56423
	31.06741
	29.06754
	1.068801
	0.1246
	20
	88.59671
	51.42648
	28.30042
	1.817163
	0.697161
	20
	16.3725
	77.38788
	47.38191
	1.633279
	0.625131

	21
	90
	29
	29
	1
	0
	21
	21.02803
	39.13531
	30.20001
	1.295871
	0.404507
	21
	17.02202
	73.79276
	49.64342
	1.486456
	0.547419

	22
	154.9549
	35.88318
	19.33833
	1.855547
	0.70956
	22
	173.4573
	54.54279
	23.73816
	2.297684
	0.810583
	22
	128.0552
	55.60815
	52.72107
	1.054761
	0.101141

	23
	90
	27
	25
	1.08
	0.142661
	23
	38.32611
	44.13373
	30.89274
	1.428612
	0.510028
	23
	39.30696
	67.32397
	41.52016
	1.621477
	0.619654

	24
	180
	25
	25
	1
	0
	24
	16.7252
	50.83078
	25.91959
	1.961095
	0.739982
	24
	173.9936
	70.11243
	54.06686
	1.296773
	0.405335

	25
	90
	21
	21
	1
	0
	25
	132.8259
	42.55606
	29.49478
	1.442834
	0.519639
	25
	9.10801
	57.07234
	52.03988
	1.096704
	0.168579

	26
	90
	21
	21
	1
	0
	26
	164.0487
	34.57021
	28.78735
	1.200882
	0.306575
	26
	52.78415
	73.99494
	50.72693
	1.458691
	0.530027

	27
	90
	21
	21
	1
	0
	27
	3.30989
	40.61481
	25.67377
	1.581957
	0.600414
	27
	58.29538
	65.38861
	44.10026
	1.482726
	0.54514

	28
	90
	21
	21
	1
	0
	28
	173.3893
	36.90399
	32.28891
	1.142931
	0.234474
	28
	87.22237
	71.72582
	33.53174
	2.139043
	0.781445

	29
	90
	21
	21
	1
	0
	29
	128.1111
	44.09251
	24.72406
	1.783385
	0.68558
	29
	60.85293
	55.65475
	36.39412
	1.529224
	0.57238

	30
	90
	21
	21
	1
	0
	30
	158.3747
	42.21863
	22.25198
	1.897298
	0.722202
	30
	45.7722
	45.43579
	39.71704
	1.143987
	0.235887

	31
	90
	21
	21
	1
	0
	31
	142.0686
	41.11554
	22.08398
	1.861781
	0.711502
	31
	148.9243
	49.39362
	43.1312
	1.145195
	0.237497

	32
	90
	21
	21
	1
	0
	32
	47.83902
	41.1167
	27.07666
	1.518529
	0.566336
	32
	18.15495
	47.52719
	46.21878
	1.028309
	0.054302

	33
	90
	21
	21
	1
	0
	33
	129.5318
	40.86987
	25.48468
	1.603703
	0.611177
	33
	37.35847
	48.54047
	48.26935
	1.005617
	0.01114

	34
	90
	21
	21
	1
	0
	34
	128.4681
	37.70828
	23.94031
	1.575096
	0.596925
	34
	175.2604
	43.95087
	41.34006
	1.063154
	0.115277

	35
	90
	21
	21
	1
	0
	35
	140.4146
	34.10962
	25.70478
	1.326976
	0.432097
	35
	151.9683
	45.71753
	41.53911
	1.10059
	0.17444

	36
	90
	21
	21
	1
	0
	36
	125.7961
	35.36652
	25.10779
	1.408588
	0.495998
	36
	82.03367
	47.84668
	40.63144
	1.177578
	0.278858

	37
	90
	21
	21
	1
	0
	37
	39.52555
	34.3643
	25.33344
	1.35648
	0.456533
	37
	64.03983
	45.26376
	41.93848
	1.079289
	0.141532

	38
	90
	21
	21
	1
	0
	38
	18.26983
	40.96265
	21.81586
	1.877655
	0.716359
	38
	174.5741
	49.51202
	38.18031
	1.296795
	0.405355

	39
	90
	21
	21
	1
	0
	39
	53.73219
	37.74707
	24.50439
	1.540421
	0.578574
	39
	42.14469
	47.49261
	38.21295
	1.242841
	0.352605

	40
	90
	21
	21
	1
	0
	40
	5.85007
	35.36719
	27.32538
	1.294298
	0.403059
	40
	23.79506
	41.40527
	41.15549
	1.006069
	0.012029

	41
	90
	21
	21
	1
	0
	41
	119.2746
	35.09839
	23.70331
	1.480738
	0.543917
	41
	70.75026
	71.12579
	24.08392
	2.953248
	0.885343

	42
	90
	21
	21
	1
	0
	42
	121.1572
	38.00842
	24.0827
	1.578246
	0.598532
	42
	140.8504
	47.08212
	34.46213
	1.366199
	0.464238

	43
	90
	21
	21
	1
	0
	43
	106.9895
	31.55203
	24.38464
	1.293931
	0.40272
	43
	95.05094
	54.11801
	33.75896
	1.603071
	0.61087

	44
	90
	21
	21
	1
	0
	44
	170.2384
	30.29196
	26.20813
	1.155823
	0.251456
	44
	51.90938
	45.57629
	44.14996
	1.032306
	0.061611

	45
	90
	21
	21
	1
	0
	45
	178.6326
	34.7868
	22.92625
	1.517335
	0.565653
	45
	43.94479
	59.08084
	38.12906
	1.549496
	0.583496

	46
	90
	21
	21
	1
	0
	46
	90.38853
	31.90491
	22.79306
	1.399764
	0.489624
	46
	52.11748
	53.80267
	39.15356
	1.374145
	0.470416

	47
	90
	21
	21
	1
	0
	47
	47.80051
	29.42792
	25.68712
	1.145629
	0.238076
	47
	19.88452
	42.05499
	32.59045
	1.290408
	0.399455

	48
	180
	21
	19
	1.105263
	0.181406
	48
	133.3025
	36.03748
	17.85168
	2.018716
	0.754614
	48
	178.506
	39.36648
	39.17914
	1.004782
	0.009495

	49
	180
	21
	19
	1.105263
	0.181406
	49
	170.071
	27.01971
	24.01302
	1.125211
	0.210173
	49
	90.69621
	40.82074
	36.99945
	1.10328
	0.17846

	50
	90
	21
	19
	1.105263
	0.181406
	50
	113.0707
	30.54202
	24.96103
	1.223588
	0.332072
	50
	92.60884
	47.97699
	41.80762
	1.147566
	0.240645

	51
	180
	21
	19
	1.105263
	0.181406
	51
	149.5027
	34.77965
	20.64371
	1.684758
	0.64769
	51
	100.2121
	47.16965
	37.12048
	1.270718
	0.380699

	52
	180
	21
	19
	1.105263
	0.181406
	52
	28.17586
	31.2254
	22.06491
	1.415161
	0.500669
	52
	102.7738
	43.30914
	31.63086
	1.369205
	0.466588

	53
	180
	21
	19
	1.105263
	0.181406
	53
	58.52135
	31.12744
	22.06354
	1.410809
	0.497584
	53
	15.26862
	39.66937
	34.75952
	1.141252
	0.23222

	54
	90
	21
	19
	1.105263
	0.181406
	54
	121.0042
	28.84711
	20.73808
	1.391021
	0.483188
	54
	99.71647
	49.11459
	27.19019
	1.806335
	0.693519

	55
	180
	21
	19
	1.105263
	0.181406
	55
	78.58969
	28.77379
	23.01257
	1.250351
	0.360359
	55
	9.26252
	36.05444
	33.49344
	1.076463
	0.137017

	56
	180
	21
	19
	1.105263
	0.181406
	56
	33.43822
	27.77856
	22.99219
	1.208174
	0.31492
	56
	2.68695
	48.85297
	37.83066
	1.291359
	0.400339

	57
	90
	21
	19
	1.105263
	0.181406
	57
	129.8357
	30.01188
	21.60541
	1.389091
	0.481751
	57
	168.3995
	47.00867
	25.96164
	1.810697
	0.694994

	58
	90
	21
	19
	1.105263
	0.181406
	58
	16.58392
	29.41595
	20.78284
	1.415396
	0.500835
	58
	72.61831
	55.30713
	39.09613
	1.414645
	0.500305

	59
	90
	21
	19
	1.105263
	0.181406
	59
	143.2109
	28.32477
	19.97998
	1.417658
	0.502426
	59
	17.26376
	38.73676
	33.71826
	1.148836
	0.242324

	60
	180
	21
	19
	1.105263
	0.181406
	60
	148.8864
	26.375
	22.79016
	1.157298
	0.253362
	60
	6.9045
	36.12372
	31.91074
	1.132024
	0.219651

	61
	180
	21
	19
	1.105263
	0.181406
	61
	41.03456
	25.67261
	21.73682
	1.181066
	0.283111
	61
	86.89257
	46.65771
	24.90759
	1.873233
	0.715019

	62
	180
	21
	19
	1.105263
	0.181406
	62
	152.1994
	31.39264
	20.18785
	1.555026
	0.586453
	62
	42.79077
	35.73334
	28.66492
	1.246588
	0.356492

	63
	180
	21
	19
	1.105263
	0.181406
	63
	159.5077
	34.80823
	15.7805
	2.205775
	0.794469
	63
	26.26138
	47.81459
	26.96988
	1.772888
	0.681846

	64
	90
	21
	19
	1.105263
	0.181406
	64
	170.2187
	25.12958
	23.06224
	1.089642
	0.157766
	64
	103.7515
	42.14136
	31.43471
	1.3406
	0.443581

	65
	180
	21
	19
	1.105263
	0.181406
	65
	152.0996
	41.12445
	13.41328
	3.06595
	0.893618
	65
	34.97627
	47.44757
	26.47437
	1.792208
	0.688668

	66
	180
	21
	19
	1.105263
	0.181406
	66
	104.6625
	31.25232
	17.33408
	1.802941
	0.692364
	66
	71.50314
	35.07794
	31.7999
	1.103083
	0.178167

	67
	90
	21
	19
	1.105263
	0.181406
	67
	178.242
	36.32611
	17.70447
	2.051804
	0.762465
	67
	64.38512
	37.64264
	24.53192
	1.534435
	0.57528

	68
	180
	21
	19
	1.105263
	0.181406
	68
	111.8664
	30.88062
	21.67929
	1.424429
	0.507146
	68
	90.84727
	42.29651
	32.6405
	1.295829
	0.404469

	69
	180
	21
	19
	1.105263
	0.181406
	69
	120.7485
	30.08057
	17.96509
	1.67439
	0.643314
	69
	63.19698
	50.49133
	25.36548
	1.990553
	0.747621

	70
	90
	21
	19
	1.105263
	0.181406
	70
	92.41044
	27.20206
	16.39128
	1.659545
	0.636903
	70
	1.01415
	56.85358
	28.20873
	2.01546
	0.753821

	71
	90
	19
	19
	1
	0
	71
	107.5166
	27.10895
	18.93354
	1.431795
	0.512204
	71
	96.27859
	34.42548
	31.31636
	1.099281
	0.172472

	72
	90
	19
	19
	1
	0
	72
	139.8837
	24.71625
	21.27856
	1.161557
	0.258827
	72
	139.4407
	36.55011
	27.05398
	1.351007
	0.452121

	73
	90
	19
	19
	1
	0
	73
	69.59625
	24.3573
	22.1067
	1.101806
	0.176261
	73
	80.51788
	40.30862
	30.14548
	1.337136
	0.440695

	74
	90
	19
	19
	1
	0
	74
	12.93845
	27.50323
	18.01758
	1.526466
	0.570834
	74
	44.59735
	37.00238
	25.30162
	1.462451
	0.53244

	75
	90
	19
	19
	1
	0
	75
	48.752
	23.91199
	18.51648
	1.29139
	0.400367
	75
	125.6044
	33.10406
	26.82913
	1.233885
	0.343174

	76
	90
	19
	19
	1
	0
	76
	113.1076
	27.61508
	21.31696
	1.295451
	0.404121
	76
	107.3292
	39.08447
	36.98117
	1.056875
	0.104732

	77
	90
	19
	19
	1
	0
	77
	42.38636
	25.32678
	21.73125
	1.165454
	0.263777
	77
	58.21991
	41.59238
	21.90958
	1.898365
	0.722514

	78
	90
	19
	19
	1
	0
	78
	31.49225
	24.74197
	20.41583
	1.211901
	0.319128
	78
	24.19505
	37.0473
	26.17291
	1.415483
	0.500896

	79
	90
	19
	19
	1
	0
	79
	170.0638
	24.552
	19.84247
	1.237346
	0.346843
	79
	27.81589
	33.12042
	24.07477
	1.375732
	0.471637

	80
	90
	19
	19
	1
	0
	80
	35.69345
	23.66492
	19.29776
	1.226304
	0.335027
	80
	159.4036
	31.56
	25.37943
	1.243527
	0.35332

	81
	90
	19
	19
	1
	0
	81
	72.23466
	25.1665
	19.14377
	1.314605
	0.421359
	81
	177.6395
	43.56567
	19.73094
	2.207988
	0.794881

	82
	90
	19
	19
	1
	0
	82
	133.7856
	28.78787
	16.4502
	1.750001
	0.67347
	82
	151.8556
	33.28784
	21.33197
	1.560467
	0.589332

	83
	90
	19
	19
	1
	0
	83
	10.66128
	26.97375
	20.42979
	1.320315
	0.426352
	83
	89.4077
	34.1684
	21.28995
	1.604907
	0.61176

	84
	90
	19
	19
	1
	0
	84
	31.79601
	24.03906
	21.56116
	1.114924
	0.195531
	84
	110.8897
	32.93036
	30.12759
	1.09303
	0.16298

	85
	90
	19
	19
	1
	0
	85
	165.7826
	22.74225
	19.28241
	1.17943
	0.281121
	85
	118.4762
	34.49258
	22.30521
	1.546391
	0.581822

	86
	90
	19
	19
	1
	0
	86
	144.0112
	24.08295
	19.1693
	1.256329
	0.366432
	86
	129.3726
	28.72668
	24.07339
	1.193296
	0.297731

	87
	90
	19
	19
	1
	0
	87
	70.26888
	22.67529
	19.51391
	1.162006
	0.259401
	87
	67.49991
	29.52859
	25.0087
	1.180733
	0.282707

	88
	90
	19
	19
	1
	0
	88
	1.34867
	26.92285
	17.22913
	1.562635
	0.590471
	88
	89.68797
	33.82422
	20.00949
	1.690409
	0.650042

	89
	90
	19
	19
	1
	0
	89
	88.20458
	22.50195
	18.31164
	1.228833
	0.337762
	89
	17.80777
	34.88794
	22.51675
	1.549422
	0.583456

	90
	90
	19
	19
	1
	0
	90
	151.973
	26.83673
	16.48256
	1.628189
	0.622784
	90
	79.70654
	29.4679
	23.17233
	1.271685
	0.381641

	91
	90
	19
	19
	1
	0
	91
	47.55389
	28.03931
	14.23148
	1.970231
	0.742388
	91
	23.15711
	28.06052
	22.00922
	1.274944
	0.384798

	92
	90
	19
	19
	1
	0
	92
	29.88286
	24.08221
	17.33629
	1.389121
	0.481773
	92
	166.3697
	26.43042
	24.39044
	1.083639
	0.148409

	93
	90
	19
	19
	1
	0
	93
	2.96804
	28.23376
	15.00635
	1.881454
	0.717504
	93
	107.1958
	32.01746
	23.70406
	1.350716
	0.451885

	94
	90
	19
	19
	1
	0
	94
	149.9662
	22.16385
	18.24049
	1.215091
	0.322698
	94
	104.7084
	26.6609
	23.07306
	1.155499
	0.251036

	95
	90
	19
	19
	1
	0
	95
	130.7258
	26.05023
	15.51627
	1.678898
	0.645226
	95
	88.36651
	34.76318
	18.89877
	1.839441
	0.704452

	96
	90
	19
	19
	1
	0
	96
	158.7375
	22.22939
	17.18427
	1.293589
	0.402405
	96
	62.33725
	29.01587
	23.01056
	1.260981
	0.371098

	97
	90
	19
	19
	1
	0
	97
	174.1003
	24.32178
	17.81512
	1.365232
	0.463479
	97
	21.37976
	31.62088
	27.47211
	1.151018
	0.245193

	98
	90
	19
	19
	1
	0
	98
	144.2268
	22.79532
	20.37633
	1.118716
	0.200975
	98
	80.71279
	24.23804
	22.36069
	1.083958
	0.14891

	99
	90
	19
	19
	1
	0
	99
	28.42448
	21.953
	21.5397
	1.019188
	0.037299
	99
	125.5402
	28.89008
	24.03259
	1.202121
	0.308004

	100
	90
	19
	19
	1
	0
	100
	170.331
	31.24695
	17.11553
	1.825649
	0.699969
	100
	72.25814
	29.80364
	20.9675
	1.421421
	0.505058

	101
	178.5051
	19.12396
	17.12465
	1.11675
	0.19816
	101
	129.2939
	22.88388
	18.46937
	1.239018
	0.348604
	101
	100.0531
	27.65741
	18.01392
	1.535335
	0.575778

	102
	178.5051
	19.12396
	17.12463
	1.116752
	0.198162
	102
	41.89371
	23.63181
	15.09569
	1.565467
	0.591951
	102
	61.4824
	28.40031
	18.93353
	1.500001
	0.555556

	103
	178.5051
	19.12396
	17.12469
	1.116748
	0.198156
	103
	138.5616
	22.52725
	16.29852
	1.382165
	0.476544
	103
	65.54389
	30.18732
	18.22073
	1.656757
	0.63568

	104
	178.5051
	19.12396
	17.12469
	1.116748
	0.198156
	104
	111.3367
	25.32971
	19.06757
	1.328418
	0.43333
	104
	62.42252
	32.47778
	17.45689
	1.860456
	0.711091

	105
	178.5051
	19.12396
	17.12465
	1.11675
	0.19816
	105
	51.20837
	21.56519
	14.14334
	1.524759
	0.569872
	105
	149.0001
	25.26477
	20.24434
	1.247992
	0.357939

	106
	90
	19
	17
	1.117647
	0.199446
	106
	29.33712
	21.26007
	17.11349
	1.242299
	0.352041
	106
	125.4371
	35.6709
	13.81649
	2.581763
	0.849974

	107
	90
	19
	17
	1.117647
	0.199446
	107
	150.5022
	25.62964
	17.97424
	1.42591
	0.508169
	107
	78.12807
	25.22571
	22.31971
	1.130199
	0.217129

	108
	90
	19
	17
	1.117647
	0.199446
	108
	85.19893
	19.82104
	15.45038
	1.282884
	0.392389
	108
	87.94746
	27.16299
	17.67688
	1.536639
	0.576497

	109
	90
	17
	17
	1
	0
	109
	34.967
	23.96985
	14.38058
	1.666821
	0.640067
	109
	106.1202
	30.23764
	18.99467
	1.591901
	0.60539

	110
	90
	17
	17
	1
	0
	110
	62.4528
	21.19739
	15.63202
	1.356024
	0.456167
	110
	127.1258
	26.01476
	17.17218
	1.514936
	0.564276

	111
	90
	17
	17
	1
	0
	111
	121.8317
	20.26462
	18.60638
	1.089122
	0.156963
	111
	119.4336
	25.49037
	18.95129
	1.345047
	0.447254

	112
	90
	17
	17
	1
	0
	112
	41.51951
	22.94019
	15.40411
	1.489225
	0.549101
	112
	106.3239
	21.89426
	19.698
	1.111497
	0.190562

	113
	90
	17
	17
	1
	0
	113
	114.1257
	21.93323
	17.96257
	1.221052
	0.329295
	113
	105.6152
	26.7525
	23.83517
	1.122396
	0.206206

	114
	90
	17
	17
	1
	0
	114
	163.6127
	19.48364
	17.90137
	1.088388
	0.155825
	114
	85.82309
	29.53583
	14.66556
	2.013959
	0.753453

	115
	90
	17
	17
	1
	0
	115
	138.8325
	19.67664
	16.4481
	1.196287
	0.301237
	115
	118.1331
	22.81378
	20.60083
	1.10742
	0.184592

	116
	90
	19
	15
	1.266667
	0.376731
	116
	25.94465
	24.66962
	13.5946
	1.814663
	0.696326
	116
	91.15097
	24.94812
	16.7742
	1.487291
	0.547928

	117
	90
	19
	15
	1.266667
	0.376731
	117
	158.5195
	21.83966
	17.21194
	1.268867
	0.378891
	117
	62.4339
	21.56262
	19.34135
	1.114846
	0.195418

	118
	90
	17
	15
	1.133333
	0.221453
	118
	120.0836
	24.36597
	12.23029
	1.992264
	0.748055
	118
	13.49873
	26.78815
	14.56772
	1.83887
	0.704268

	119
	90
	17
	15
	1.133333
	0.221453
	119
	174.6803
	22.40778
	13.94998
	1.606295
	0.612431
	119
	172.5046
	21.84119
	15.20956
	1.436017
	0.515068

	120
	90
	15
	15
	1
	0
	120
	120.9573
	27.12358
	12.12726
	2.236579
	0.800091
	120
	132.3893
	24.76703
	19.96857
	1.240301
	0.349951

	121
	90
	15
	15
	1
	0
	121
	79.31702
	22.81976
	14.53088
	1.570432
	0.594527
	121
	44.81573
	25.8479
	11.86823
	2.177907
	0.789175

	122
	90
	15
	15
	1
	0
	122
	173.3637
	18.38602
	16.30194
	1.127842
	0.213854
	122
	109.0332
	19.60504
	16.80917
	1.16633
	0.264882

	123
	90
	15
	15
	1
	0
	123
	172.9556
	22.63751
	13.89073
	1.629685
	0.623476
	123
	4.78158
	24.52631
	13.45456
	1.822899
	0.699064

	124
	90
	15
	15
	1
	0
	124
	16.29719
	23.71362
	12.84848
	1.845636
	0.706433
	124
	136.3014
	20.07629
	18.11688
	1.108154
	0.185671

	125
	90
	15
	15
	1
	0
	125
	21.87079
	18.8727
	15.01508
	1.256916
	0.367024
	125
	127.3661
	18.04207
	15.34357
	1.175872
	0.276764

	126
	90
	15
	13
	1.153846
	0.248889
	126
	119.0316
	21.08679
	14.13959
	1.49133
	0.550373
	126
	162.7793
	19.37018
	15.01379
	1.290159
	0.399223
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