Table 1. XRF component analysis of the black sample with pillow-shaped porcelain on the left from the Sui Dynasty in Figure 1
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Table 2. XRF component analysis of the yellow samples with the bowl-shaped fragment in the middle from the Tang Dynasty in Figure 1
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Table 3. XRF component analysis of the yellow sample with the arch-shaped fragment on the right side from the Tang Dynasty in Figure 1
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Table 4. XRF component analysis of the left black dot sample from modern times in Figure 2
[image: ]






Table 5. XRF component analysis of cyan samples in the middle from modern times in Figure 2
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Table 6. XRF component analysis of yellow samples on the right side from the modern eras in Figure 2
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Compound  Concentration  Unit  

Al 2 O 3  23.234  %  

SiO 2  76.562  %  

P 2 O 5  47.2  ppm  

SO 3  23.5  ppm  

Cl  4.2  ppm  

K 2 O  644.4  ppm  

CaO  708.0  ppm  

TiO 2  579.3  ppm  

V 2 O 5  17.4  ppm  

Cr 2 O 3  4.7  ppm  

MnO  19.4  ppm  
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Compound  Concentration  Unit  

Al 2 O 3  23.487  %  

SiO 2  76.296  %  

P 2 O 5  56.0  ppm  

SO 3  45.9  ppm  

Cl  5.6  ppm  

K 2 O  810.0  ppm  

CaO  625.3  ppm  

TiO 2  586.0  ppm  

V 2 O 5  16.9  ppm  

Cr 2 O 3  4.5  ppm  

MnO  19.4  ppm  
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Compound  Concentration  unit  

Al 2 O 3  18.060  %  

SiO 2  81.772  %  

P 2 O 5  49.9  ppm  

SO 3  21.9  ppm  

Cl  4.7  ppm  

K 2 O  983.5  ppm  

CaO  609.7  ppm  

TiO 2  453.4  ppm  

V 2 O 5  10.7  ppm  

Cr 2 O 3  3.7  ppm  

MnO  36.8  p pm  

SnO 2  0.9  ppm  
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Compound  Conc  Unit  

Al 2 O 3  15.804  ％  

SiO 2  83.940  ％  

P 2 O 5  102.6  ppm  

SO 3  6.7  ppm  

Cl  8.4  ppm  

K 2 O  0.142  ％  

CaO  667.4  ppm  

TiO 2  308.3  ppm  

V 2 O 5  7.5  ppm  

Cr 2 O 3  2.4  ppm  

MnO  42.1  ppm  


image5.emf
 

Compound  Conc  Unit  

Al 2 O 3  18.918  ％  

SiO 2  80.770  ％  

SO 3  8.2  ppm  

Cl  6.3  ppm  

K 2 O  0.159  ％  

CaO  0.123  ％  

TiO 2  229.0  ppm  

V 2 O 5  4.4  ppm  

Cr 2 O 3  1.6  ppm  

MnO  42.6  ppm  
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Compound  Conc  Unit  

Al 2 O 3  17.899  ％  

SiO 2  81.867  ％  

SO 3  8. 6  ppm  

Cl  7.6  ppm  

K 2 O  0.147  ％  

CaO  776.2  ppm  

TiO 2  47.9  ppm  

V 2 O 5  1.0  ppm  

Cr 2 O 3  0.4  ppm  

MnO  34.5  ppm  


