Supplementary information

Vanadium oxide-doped laser-induced graphene multi-parameter sensor to decouple soil nitrogen loss and temperature

Li Yang1, *, Jiayi Yan3, Chuizhou Meng3, Ankan Dutta2, Xue Chen4, Ye Xue1, Guangyu Niu5, Ya Wang3, Shuaijie Du4, Huanyu Cheng2, *.

1 State Key Laboratory of Reliability and Intelligence of Electrical Equipment, School of Health Sciences and Biomedical Engineering, Hebei University of Technology, Tianjin, 300130, China.

2 Department of Engineering Science and Mechanics, The Pennsylvania State University, University Park, 16802, USA.

3 State Key Laboratory for Reliability and Intelligence of Electrical Equipment, Hebei Key Laboratory of Smart Sensing and Human-Robot Interaction, School of Mechanical Engineering, Hebei University of Technology, Tianjin, 300401, China.

4 State Key Laboratory of Reliability and Intelligence of Electrical Equipment, Key Laboratory of Bioelectromagnetics and Neuroengineering of Hebei Province, School of Electrical Engineering, Hebei University of Technology, Tianjin, 300130, China.

5School of Architecture and Art, Hebei University of Technology, Tianjin, 300130, China.

*Corresponding author. E-mail: yangli5781@126.com; huanyu.cheng@psu.edu

Fig. S1. Schematic illustration showing the fabrication process of the multi-parameter sensor.

Fig. S2. The film thickness as a function of spin coating speed.

Fig. S3. Optical images of a pure F127-Resol film, b V5S8-doped F127-Resol film on a glass slide, c VOX-doped LIG sensor after laser scribing of (b), and d the VOX-doped LIG patterns prepared by the vector (top) and raster (bottom) modes.

Fig. S4. X-ray photoelectron spectroscopy (XPS) spectra of V-2p for VOX-doped LIG with a zoom-in shown.

Fig. S5. Infrared images showing the spatial distribution of the temperature in the sensing region from different self-heating conditions: a 20.2℃, b 30.1℃, c 40.7℃, and d 50.3℃.

Fig. S6. The typical response curve showing the calculation of response and recovery times of the VOX-doped LIG gas sensor to 1 ppm NO2 at 30ºC.

Fig. S7. Response curve of VOX-doped LIG sensor under different operating humidity at room temperature.

Fig. S8. Response curves of the VOX-doped LIG sensor to 1 ppm NO2 under different operating relative humidity at 50℃.

Fig. S9. Current-voltage (I-V) curves of pure LIG and VOX-doped LIG sensors.

Fig. S10. Linear fit of the resistance change in the VOX-doped LIG sensor with the temperature from 30 to 50ºC.

Fig. S11. Comparison in the VOX-doped LIG sensor response to 30, 40, and 50°C between the sensors with different film thickness encapsulation layer.

Fig. S12. Temperature region of the VOX-doped LIG sensor in decoupling experiment.

Fig. S13. The difference in the sensor response to different fertilizer levels at room temperature.

Tab. S1. Performance comparison between our VOX-doped LIG sensor and other NO2 gas sensors.

| Materials | Synthesis Method | Demonstrated LOD |  | Temperature (℃) | Response/recovery Time (s) |  | Calculated LOD |  | Interference gases used for selectivity | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| V2O5/graphene | Deposition |  | 1 ppm | RT | 19/29 (100 ppm) | — |  | CO2 |  | 1 |
| Porous silicon /V2O5 | Galvanostatic electrochemical etching method + deposition |  | 250 ppb | RT | 60/450 (3 ppm) | — |  | NH3, acetone, methanol, methanol |  | 2 |
| Gold black/VOX | Radio frequency magnetron sputtering and low-temperature vapor cooling condensation |  | 1 ppm | 270 | 181/183 (1 ppm) | — |  | C2H6O, NH3 |  | 3 |
| V2O5 nanorods | Chemical spray pyrolysis |  | 10 ppm | 200 | 20/150 (100 ppm) | — |  | — |  | 4 |
| V2O5 nanoislands /SnO2 nanowires | Atomic layer deposition (ALD) and thermal post-treatment |  | 50 ppb | 250 | 300/850 (5 ppm) | 139 ppt |  | C2H5OH, SO2, CHCOCH, H2, H2S, C7H8, C6H6, and CO |  | 5 |
| VO2 nanowire | Chemical vapor deposition |  | 1 ppm | RT | 30/210 (1 ppm) | — |  | CH3CHOHCH3, NH3, CHCOCH, and C2H5OH |  | 6 |
| V2O5 nanocolumn | Glancing angle deposition |  | — | 150 | 500/583 (5ppm) | — |  | C2H5OH, CO, CH4, SO2 |  | 7 |
| VO2 nanosheet | Hydrothermal method |  | 500 ppb | RT | 55/270 (5 ppm) | 20 ppb |  | SO2, ethanol, acetone, methanol, NH3 |  | 8 |
| MoS2@rGO | solvothermal method |  | 10 ppb | RT | 360/720 (1 ppm) | 4.4 ppb |  | SO2, CO, NH3, NO, C2H5OH, (CH3)2CO |  | 9 |
| MoS2/LIG | Laser induction and dripping |  | 250 ppb | 150 | 1200/1800 (2 ppm) | 317 ppt |  | H2S, SO2, CO, NH3, NO |  | 10 |
| LIG-rGO/MoS2 | Laser induction |  | 10 ppb | Self-heating | 360/720 (1 ppm) | 1.2 ppb |  | NH3, NO, SO2, CO, CH3COCH3, C2H5OH, CH3OH |  | 11 |
| n‑SnSe2/p-SnO/n-SnSe | Hydrothermal method |  | 1 ppm | RT | 34/272 (5 ppm) | 115 ppb |  | SO2, NH3, C2H5OH, H2, NO, CO, H2S |  | 12 |
| VOX/LIG | Laser one-step preparation |  | 3 ppb | RT | 217/650 (1 ppm) | 451 ppt |  | NO, NH3, SO2, CH3OH, C2H5OH, CHCOCH, H2S |  | This work |

Tab. S2. Performance comparison between our VOX-doped LIG sensor and other temperature sensors.

| Materials | Synthesis Method | LOD (℃) | Range (℃) | Reference |
| --- | --- | --- | --- | --- |
| VOX | Deposition | 1 | 20-57 | 13 |
| VO2 | Atomic layer deposition | — | 25-65 | 14 |
| Ionic gel/PVA | Shadow mask and transfer printing | — | 30-80 | 15 |
| Pt/PI | Deposition and laser induction | 1 | 20-45 | 16 |
| PANI NF | Two-step method | 2.7 | 40-110 | 17 |
| Reduced graphene oxide | Spin-coating method and lamination techniques | 0.2 | 30-80 | 18 |
| Graphene/NC composite | Liquid exfoliation method | 2.5 | 100-400 | 19 |
| Graphene | Deposition | 10 | 20-100 | 20 |
| MWCNT | Dispensing printing technology | — | 20-300 | 21 |
| Si/SiO2-substrate graphene | Chemical vapor deposition | 10 | 70-120 | 22 |
| PEDOT:PSS/PDMS | Drop-casting | 0.1 | 5-55 | 23 |
| Cu-CuNi/ Kapton | Printing | 5 | 30-140 | 24 |
| Silk/PEDOT:PSS | Photolithography | 5 | 20-50 | 25 |
| VOX/LIG | Laser one-step preparation | 0.2 | 10-110 | This work |

REFERENCES

- Chavez, D., Gomez-Solis, C., Mtz-Enriquez, A. I., Rodriguez-Gonzalez, V., Escobar-Barrios, V., Garcia, C. R., Oliva, J. High Sensitivity of Flexible Graphene Composites Decorated with V2O5 microbelts for NO2 detection. Mater. Res. Bull. 133, 111052 (2020).

- Yan, W., Hu, M., Wang, D., Li, C. Room temperature gas sensing properties of porous silicon/V2O5 nanorods composite. Appl. Surf. Sci. 346, 216-222 (2015).

- Yeh, T. H., Chu, S. Y., Lee, H. Y., Lee, C. T. Performance improvement of nitrogen dioxide gas sensors based on novel p-n heterojunction gold black/VOX bi-sensing membranes. Mater. Sci. Semicond. Process. 115, 105125 (2020).

- Mane, A. A., Moholkar, A. V. Effect of film thickness on NO2 gas sensing properties of sprayed orthorhombic nanocrystalline V2O5 thin films. Appl. Surf. Sci. 416, 511-520 (2017).

- Ko, W. C., Kim, K. M., Kwon, Y. J., Choi, H., Park, J. K., Jeong, Y. K., ALD-assisted synthesis of V2O5 nanoislands on SnO2 nanowires for improving NO2 sensing performance. Appl. Surf. Sci. 509, 144821 (2020).

- Liang, J., Zhao, Y., Zhu, K., Guo, J., Zhou, L. Synthesis and room temperature NO2 gas sensitivity of vanadium dioxide nanowire structures by chemical vapor deposition. Thin Solid Films 669, 537-543 (2019).

- Han, S. D., Moon, H. G., Noh, M. S., Pyeon, J. J., Shim, Y. S., Nahm, S., Kim, J. S., Yoo, K. S., Kang, C. Y. Self-doped nanocolumnar vanadium oxides thin films for highly selective NO2 gas sensing at low temperature. Sens. Actuators, B 241, 40-47 (2017).

- Liang, J., Lou, Q., Wu, W., Wang, K., Xuan, C. NO2 Gas Sensing Performance of a VO2(B) Ultrathin Vertical Nanosheet Array: Experimental and DFT Investigation. ACS Appl. Mater. Interfaces 13, 31968-31977 (2021).

- Yi, N., Cheng, Z., Li, H., Yang, L., Zhu, J., Zheng, X., Chen, Y., Liu, Z., Zhu, H., Cheng, H. Stretchable, ultrasensitive, and low-temperature NO2 sensors based on MoS2@rGO nanocomposites. Mater. Today Phys. 15, 100265 (2020).

- Peng, Z., Tao, L., Zou, S., Zhu, C., Wang, G., Sun, H., Ren, T. A Multi-functional NO2 gas monitor and Self-Alarm based on Laser-Induced graphene. Chem. Eng. J. 428, 131079 (2022).

- Yang, L., Yi, N., Zhu, J., Cheng, Z., Yin, X., Zhang, X., Zhu, H. L., Cheng H. Novel gas sensing platform based on a stretchable laser-induced graphene pattern with self-heating capabilities. J. Mater. Chem. A 8, 6487-6500 (2020).

- Rani, S., Kumar, M., Garg, P., Parmar, R., Kumar, A., Singh, Y., Baloria, V., Deshpande, U., Singh, V. N. Temperature-Dependent n-p-n Switching and Highly Selective Room-Temperature n-SnSe2/p-SnO/n-SnSe Heterojunction-Based NO2 Gas Sensor. ACS Appl. Mater. Interfaces 14, 15381-15390 (2022).

- Billard, M. W., Basantani, H. A., Horn, M. W., Gluckman, B. J. A Flexible Vanadium Oxide Thermistor Array for Localized Temperature Field Measurements in Brain. IEEE Sens. J. 16, 2211-2212 (2016).

- Muller, A. A., Khadar, R., Niang, K. M., Bai, G. D., Matioli, E., Robertson, J., Ionescu, A. M. in 2021 21st International Conference on Solid-State Sensors, Actuators and Microsystems (Transducers). 1355-1358 (2021).

- Yamada, S., Toshiyoshi, H. Temperature Sensor with a Water-Dissolvable Ionic Gel for Ionic Skin. ACS Appl. Mater. Interfaces 12, 36449-36457 (2020).

- Kang, S., Naqi, M., Shin, J., Lee, S., Lee, M., Gandla, S., Kim. S. Laser-Processed Stretchable-Gradient Interconnection-Based Temperature Sensor for a Real-Time Monitoring System. ACS Appl. Mater. Interfaces 3, 5601-5607 (2021).

- Ge, G., Lu, Y., Qu, X., Zhao, W., Ren, Y., Wang, W., Wang, Q., Huang, W., Dong, X. Muscle-Inspired Self-Healing Hydrogels for Strain and Temperature Sensor. ACS Nano 14, 218-228 (2020).

- Trung, T. Q., Ramasundaram, S., Hwang, B. U., Lee, N. E. An All-Elastomeric Transparent and Stretchable Temperature Sensor for Body-Attachable Wearable Electronics. Adv. Mater. 28, 502-509 (2016).

- Wei, W., Yi, Y., Song, J., Chen, X., Li, J., Li, J. Tunable Graphene/Nitrocellulose Temperature Alarm Sensors. ACS Appl. Mater. Interfaces 14, 13790-13800 (2022).

- Štulík, J., Musil, O., Josefík, F., Kadlec, P. Graphene-Based Temperature Sensors-Comparison of the Temperature and Humidity Dependences. Nanomaterials 12 (2022).

- Peng, X., Zhang, X., Wang, R., Chen, Y., Chu, X., Kong, L., Yan, X., Kuang, M. Printing of Carbon Nanotube-Based Temperature and Bending Sensors for High-Temperature-Resistant Intelligent Textiles. ACS Appl. Electron. Mater. 4, 1949-1957 (2022).

- Liu, D., Chen, S., Lu, Z., Ma, N., Sun, Y. Temperature sensor based on temperature and frequency dependence of graphene impedance. J. Phys. D: Appl. Phys. 52, 075102 (2018).

- Yu, Y., Peng, S., Blanloeuil, P., Wu, S., Wang, C. H. Wearable Temperature Sensors with Enhanced Sensitivity by Engineering Microcrack Morphology in PEDOT:PSS-PDMS Sensors. ACS Appl. Mater. Interfaces 12, 36578-36588 (2020).

- Rahman, M. T., Cheng, C. Y., Karagoz, B., Renn, M., Schrandt, M., Gellman, A., Panat,. R. High Performance Flexible Temperature Sensors via Nanoparticle Printing. ACS Appl. Nano Mater. 2, 3280-3291 (2019).

- Pradhan, S., Yadavalli, V. K. Photolithographically Printed Flexible Silk/PEDOT:PSS Temperature Sensors. ACS Appl. Electron. Mater. 3, 21-29 (2021).