Water-Soluble Supramolecular Polymers Driven by Naphthalene-Naphthalene Interaction

By Weijian Xue*, Huiqian Li, Ying Zhang, Yang Liu, Bing Zhao, Xiangfeng Guo

Heilongjiang Provincial Key Laboratory of Surface Active Agent and Auxiliary, College of Chemistry and Chemical Engineering, Qiqihar University, Qiqihar 161006, PR China

Supporting Information

| Table of contents | Pages |
| --- | --- |
| General experimental details | S2 |
| Synthetic procedures and characterization data 1H and 13C NMR spectra of new compounds 1H NMR spectra of selected guest 3 with hosts 1 and 2 | S3-S4 S5-S8 S9-S10 |
| DLS of 2 in water at variable concentrations | S11 |
| NOESY spectrum of 1 and 2 | S12-S13 |
| Fluorescence spectra of 1 and 2 in water | S14-S15 |
| 1H NMR dilution studies for 1 | S16 |

* To Whom Correspondence should be addressed.

Email: hehexueweijian@163.com

General experimental details

Starting materials were purchased from commercial suppliers and were used without further purification. 1H NMR and 13C NMR spectra were recorded on a Bruker AVANCE-600 spectrometer and referenced to internal tetramethylsilane. Infrared spectral data were measured with Nicolet Avatar-370. Mass spectra were obtained on a Waters Xevo G2-S QT. Melting points were measured using an X-6 microscopic melting point apparatus (Beijing, China). The UV–vis spectra were measured on a Puxi TU-1901 (Beijing, China) spectrophotometer. Fluorescence measurements were made on a Hitachi F-7000 (Tokyo, Japan). Dynamic light scattering (DLS) experiments were performed on a Zetasizer Nano ZS90. The Scanning Electron Microscope (SEM) images were obtained on Hitachi SU8010microscope. AFM images were obtained on a Multi Mode 8 instrument.

References:

1) R. Gornpper, H. Noth., W. Rattay, M. Schwarzensteiner, P. Spes, H. Wagner, Anqew Chem Int Ed Engl. 1987, 26, 1039-1041.

2) a) D. Ma, G. Hettiarachchi, D. Nguyen, B. Zhang, J. B. Wittenberg, P. Y. Zavalij, V. Briken, L. Isaacs, Nat. Chem. 2012, 4, 503-510.  b) Zhang, B.; Zavalij, P. Y.; Isaacs, L., Org. Biomol. Chem. 2014, 12, 2413-2422.

Synthetic procedures and characterization data

Scheme S1. Synthetic procedures of Compounds 1 and 2

Compounds 1 and 2 were synthesized according to Scheme S1. Naphthalene substituted glycoluril was synthesized in toluene in good yield.[1] The desired monomer 1 and its analogue 2 were synthesized by using TFA as solvent in good yield.[2]

Compound 1. A solution of 4 (350 mg, 1 mmol) in TFA (10 mL) was treated with benzene wall prepared from the reference 2 (1.59 g, 4 mmol). The mixture was stirred and heated at 90 ˚C for 3 h. The solvent was removed by rotary evaporation and the solid was dried in high vacuum. The solid was washed with the mixture of water and acetone (1:2, v/v, 10 mL × 2). The solid was dissolved in water (10 mL) and adjusted to pH = 7 by adding 1 M aqueous NaOH. The solvent was removed by rotary evaporation and then the solid was further dried under high vacuum to yield 1 as a white solid (200 mg, 18%). M.p. > 318 oC (decomposed). IR (ATR, cm-1): 3454w, 2923m, 1690s, 1645m, 1466s, 1437m, 1263m, 1194s, 1049s, 882m, 815m, 616m. 1H NMR (600 MHz, D2O): 7.94 (d, J = 7.2, 2H), 7.87 (d, J = 8.4, 2H), 7.67 (t, J = 7.2, 2H), 6.89 (s, 4H), 5.41 (d, J = 16.2, 4H), 4.71 (d, J = 16.2, 4H), 4.08 (m, 8H), 3.10 (m, 8H), 2.20 (m, 8H). 13C NMR (125 MHz, D2O, ethanol as internal reference): δ 158.1, 150.9, 138.1, 136.4, 132.5, 129.1, 128.8, 127.1, 120.5, 115.6, 85.9, 69.4, 48.7, 36.9, 25.2. MS (ESI): m/z 1087. 9328 ([M - Na]-), calculated 1088.1109, m/z 532.2291 ([M - 2Na]2-), calculated 532.5608, m/z 347.0428 ([M - 3Na]3-), calculated 347.3775.

Compound 2. A solution of 4 (350 mg, 1 mmol) in TFA (10 mL) was treated with Naphthalene wall prepared from the reference 2 (1.79 g, 4 mmol). The mixture was stirred and heated at 90 ˚C for 3 h. The solvent was removed by rotary evaporation and the solid was dried in high vacuum. The solid was washed with the mixture of water and acetone (1:2, v/v, 10 mL × 2). The solid was dissolved in water (10 mL) and adjusted to pH = 7 by adding 1 M aqueous NaOH. The solvent was removed by rotary evaporation and then the solid was further dried under high vacuum to yield 2 as a dark purple solid (250 g, 20%). M.p. > 306 oC (decomposed). IR (ATR, cm-1): 3463w, 2933m, 1688s, 1639m, 1461s, 1426m, 1348m, 1193s, 1042s, 852m, 814m, 777m. 1H NMR (600 MHz, D2O): 7.82 (s, 4H), 7.46 (s, 4H), 7.27 (s, 2H), 7.04 (s, 4H), 5.60 (d, J = 15.6, 4H), 4.93 (d, J = 15.6, 4H), 4.20 (d, J = 9.0, 4H), 3.97 (d, J = 7.8, 4H), 3.22 (m, 8H), 2.35 (m, 8H). 13C NMR (125 MHz, D2O, ethanol as internal reference): δ 157.7, 149.5, 137.3, 135.7, 131.9, 128.2, 127.9, 127.4, 126.7, 126.5, 122.3, 119.3, 84.9, 74.8, 48.8, 48.6, 37.9, 25.9. MS (ESI): m/z 1187. 3946 ([M - Na]-), calculated 1187. 1388, m/z 582.2559 ([M - 2Na]2-), calculated 582.0748, m/z 380.3866 ([M - 3Na]3-), calculated 380.3868.

1H and 13C NMR spectra of new compounds

Figure S1. 1H NMR of 1 recorded on 600 MHz in D2O.

Figure S2. 13C NMR spectra (125 MHz, D2O, ethanol as internal reference) recorded for 1.

Figure S3. 1H NMR of 2 recorded on 600 MHz in D2O.

Figure S4. 13C NMR spectra (125 MHz, D2O, ethanol as internal reference) recorded for 2.

1H NMR spectra of selected guest 3 with hosts 1 and 2

Figure S5.  1H NMR spectra recorded (600 MHz, RT, D2O) for: (a) receptor 2 (1 mM), (b) guest 3 (1 mM), (c) 2 (1 mM) and 3 (0.5 mM), (d) 2 (1 mM) and 3 (1 mM), (e) 2 (1 mM) and 3 (1.5 mM), (f) 2 (1 mM) and 3 (2 mM), (g) 2 (1 mM) and 3 (3 mM), (h) 2 (1 mM) and 3 (4 mM).

Figure S6.  1H NMR spectra recorded (600 MHz, RT, D2O) for: (a) receptor 1 (1 mM), (b) guest 3 (1 mM), (c) 1 (1 mM) and 3 (1 mM), (d) 1 (1 mM) and 3 (2 mM).

DLS of 2 in water at variable concentrations

Figure S7. DLS of 2 in water at variable concentrations.

NOESY spectrum of 1 and 2

Figure S8. NOESY spectrum of 1 at 296 K in D2O.

Figure S9. NOESY spectrum of 2 at 296 K in D2O.

Fluorescence spectra of 1 and 2 in water

Figure S10. Fluorescence spectra in water with different concentration of 1 (10-4M, 10-5M)

Figure S11. Fluorescence spectra in water with different concentration of 2 (10-2M , 10-3M ,10-4M, 10-5M)

1H NMR dilution studies for 1

Figure S12.  1H NMR spectra recorded (600 MHz, RT, D2O) for: (a) receptor 1 (1 mM), (b) receptor 1 (10 mM).