Rational construction of NH2-UiO-66/Bi2MoO6 nanocomposite with accelerating charge transfer for enhanced visible-light photocatalytic activity

Qingsong Hua*, Zhixin Wanga, Ting Zhoua, Zhenxing Wanga, Jintao Dongb, Xingwang Zhua, Jianjian Yia, Yiqun Xua*

aCollege of Environmental Science and Engineering, Yangzhou University, 196 West Huayang Road, Yangzhou, 225127, PR China

bSchool of Chemistry and Chemical Engineering, Institute for Energy Research, Jiangsu University, 301 Xuefu Road, Zhenjiang, 212013, PR China.

*Corresponding author:

Dr. Qingsong Hu

Tel.: +86-514-87979528, Fax: +86-514-87978626

E-mail address: huqs@yzu.edu.cn

Dr. Yiqun Xu

Tel.: +86-514-87979528, Fax: +86-514-87978626

E-mail address: yqxu@yzu.edu.cn

Supplementary information

Synthesis of NH2-UiO-66

0.23 g zirconium(IV) chloride and 0.18 g 2-aminoterephthalic acid were dissolved into 50 mL N,N-dimethyl formamide (DMF) and stirred for 1 h. The mixture was then transfered into a 100 mL Teflon-lined autoclave and reacted at 120 °C for 48 h, then cooled. The obtained sample was centrifuged at high speed and washed with DMF and methanol to remove the unreacted 2-aminoterephthalic acid. The yellow liquid was suspended into methanol and stirred for 24 h to remove the residual DMF. The final product was dried under vacuum at 80 °C for 24 h.

Fig. S1. TEM images of Bi2MoO6 (a,b) and NH2-UiO-66 (c,d).

Fig. S2. XPS spectra of 5 wt% NU/BMO.

Fig. S3 Nitrogen absorption-desorption isotherms and pore diameter distribution of NH2-UiO-66.

Fig. S4. The adsorption equilibrium of RhB over different samples in the darkness.

Fig. S5. Cycling runs for RhB degradation over 5 wt% NU/BMO under visible light irradiation (a), the XRD patterns of 5 wt% NU/BMO before and after five cycles (b).

Fig. S6. (αhν)0.5 vs. hν (photon energy) curves of Bi2MoO6 and NH2-UiO-66.

Fig. S7. The Motty-Schottky plots of NH2-UiO-66 (a) and Bi2MoO6 (b).

Fig. S8. Valence-band XPS spectra of NH2-UiO-66 (a) and Bi2MoO6 (b).