Table.1. indicates all experimental parameters from Z-scan technique for PzZrOCl single crystals.

| Laser beam wavelength | 532 nm |
| --- | --- |
| Lens focal length (f) | 103 mm |
| Optical path length | 675 mm |
| Aperture radius (ra) | 1.5 mm |
| Sample thickness | 1 mm |
| Linear refractive index(n0) | 1.02475 |
| Nonlinear refractive index (n2) | 3.92×10-10 (cm2W) |
| Nonlinear absorption coefficient (β) | 5.40×10-6 (cmW) |
| Real part of the third order susceptibility Re (χ3) | 10.39×10-9(cm2W) |
| Imaginary part of the third order susceptibility Im (χ3) | 0.60×10-9 (cmW) |
| third order Nonlinear optical susceptibility (χ3) | 10.39×10-9 esu |