Supporting Information

Figure S1, Elemental ratio of biological Mn2O3(A）to Mn2O3(B) analyzed by energy dispersive X-ray spectroscopy (EDS).

Figure S2. Morphology and characterization of iron-modified biogenic MnOX: (A) X-ray photoelectron spectroscopy (XPS) spectra of Mn 2p orbitals and fitted by software Thermo Advantage (V5.948). The binding energy of the samples was calibrated by the carbon C1s binding energy (284.6 eV). (B) Scanning electron microscope (SEM) image of iron-modified biological Mn2O3. (C) XRD diffraction pattern of iron-modified biogenic MnOX. (D) X-ray photoelectron spectroscopy (XPS) spectra of Fe 2p orbitals and fitted by the software Thermo Advantage (V5.948). The binding energy of the samples was calibrated by the carbon C1s binding energy (284.6 eV).

Figure S3. Morphology and characterization of commercial Mn2O3: (A) X-ray photoelectron spectroscopy (XPS) spectra of Mn 2p orbitals and fitted by the software Thermo Advantage (V5.948). The binding energy of the samples was calibrated by the carbon C1s binding energy (284.6 eV). (B) Scanning electron microscope (SEM) image of Mn2O3. (C) XRD pattern of Mn2O3

Figure S4, UV-Vis spectrum scan of phenanthrene degradation process, (A) UV-Vis spectrum of phenanthrene degradation by biological Mn2O3 and chemical Mn2O3 catalyzed by PMS for 120 min. (B) UV-Vis spectra of bio-Mn2O3-catalyzed PMS degradation of phenanthrene at different time points.

Figure S5. Heat map of microbial communities after the PMS AOP.

Table S1.EDS element ratio table of biological Mn2O3 and Mn2O3

| Biological Mn2O3 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Element | Line type | Wt% | Wt%Sigma | At% |
| C | K line system | 21.67 | 0.40 | 41.42 |
| O | K line system | 25.42 | 0.31 | 36.48 |
| Mn | K line system | 52.90 | 0.39 | 22.10 |
| Mn2O3 |  |  |  |  |
| C | K line system | 3.80 | 0.25 | 8.92 |
| O | K line system | 33.29 | 0.21 | 58.74 |
| Mn | K line system | 62.92 | 0.25 | 32.33 |