Supplemental Information:

Tab. S1 EIS Fitted Parameters Extracted from Nyquist Plots of BiVO4, BiVO4-Ov, BiVO4/FeOOH, and BiVO4-Ov/FeOOH photoelectrodes

Table S2 Flat band potential (VFB) and carrier density (Nd) of BiVO4, BiVO4-Ov, BiVO4/FeOOH, and BiVO4-Ov/FeOOH photoelectrodes

Tab. S3 The rate constant of BiVO4-Ov/FeOOH photoelectrode degradation of RhB under different conditions

Tab. S1 EIS Fitted Parameters Extracted from Nyquist Plots of BiVO4, BiVO4-Ov, BiVO4/FeOOH, and BiVO4-Ov/FeOOH photoelectrodes

| Sample | Rs (Ω·cm2) | Rct (Ω·cm2) | CPE (F/cm2) |
| --- | --- | --- | --- |
| BiVO4 | 31.03 | 34305 | 2.23×10-5 |
| BiVO4-Ov | 29.86 | 23822 | 2.32×10-5 |
| BiVO4/FeOOH | 28.38 | 11077 | 3.56×10-5 |
| BiVO4-Ov/FeOOH | 25.47 | 8963 | 2.69×10-5 |

Table S2 Flat band potential (VFB) and carrier density (Nd) of BiVO4, BiVO4-Ov, BiVO4/FeOOH, and BiVO4-Ov/FeOOH photoelectrodes

| Sample | VFB (V vs. RHE) | Nd (cm-3) |
| --- | --- | --- |
| BiVO4 | 0.483 | 0.808×1028 |
| BiVO4-Ov | 0.461 | 2.42×1028 |
| BiVO4/FeOOH | 0.432 | 4.35×1028 |
| BiVO4-Ov/FeOOH | 0.373 | 7.84×1028 |

Tab. S3 The rate constant of BiVO4-Ov/FeOOH photoelectrode degradation of RhB under different conditions

| Conditions | Only light | Only bias potential | Light + bias potential |
| --- | --- | --- | --- |
| K·(min)-1 | 0.01069 min-1 | 0.00588 min-1 | 0.01925 min-1 |