Supplementary Information for

Solvent-free and long-cycling garnet-based lithium-metal batteries

Jiameng Yu1, Chang Zhang1, Cong Wu1, Ran Wei1, Shaojie Chen1, Yingjie He1, Qilin Hu1, Wei Liu1,2

1School of Physical Science and Technology, ShanghaiTech University, Shanghai 201210, China.

2Shanghai Key Laboratory of High-resolution Electron Microscopy, ShanghaiTech University, Shanghai 201210, China

E-mail address: liuwei1@shanghaitech.edu.cn

Supplementary Figure 1. Synthetic diagram of the preparation of (Li,K,Cs)FSI molten salt electrolyte.

Supplementary Figure 2. Phase diagram of ternary system LiFSI–KFSI–CsFSI 1.

b

c

d

a

Supplementary Figure 3. Characterization of molten salts. a XRD patterns of the LiFSI, KFSI, CsFSI and (Li,K,Cs)FSI. b SEM image of (Li,K,Cs)FSI eutectic powder. c Optical image of flame test of molten salts. d Impedance spectra of the (Li,K,Cs)FSI electrolytes held by glass fiber separator with 0.18 mm in thickness and 16 mm in diameter as the configuration of SS/ (Li,K,Cs)FSI /SS at the temperature range from 10 to 80 °C.

a

d

b

c

Supplementary Figure 4. Characterization of garnet electrolyte. a XRD patterns of the LLZTO powder and pellet. b Optical photograph of ceramic pellet and SEM morphology of LLZTO powder, pellet’s surface and across section. c Nyquist plots of the LLZTO pellet measured at the temperature range from 20 to 80 °C. d The fitted Arrhenius plot of the garnet electrolytes.

c

b

d

a

Supplementary Figure 5. Performance of Li/LLZTO/Li symmetric battery. a EIS spectra of symmetric battery tested at RT, 45 °C, 60 °C and 80 °C. b Critical current density of the Li symmetric battery at 60 °C. c,d Galvanostatic cycling performance of the Li/LLZTO/Li cells at 0.3 mA cm-2 45 °C (c) and 0.6 mA cm-2 60 °C (d) with 0.5 h for each plating/stripping half cycle and for a total cycling time of 1000 hours.

Supplementary Figure 6. Morphology of the cross section of pristine commercial cathode piece.

b

a

Supplementary Figure 7. a,b EIS spectra of LFP half cells with liquid electrolyte modification in the cathode side (a) and without any modification (b).

b

a

Supplementary Figure 8. a Rate capacity performance of LFP half cell at 80 °C. b The corresponding charge-discharge voltage profiles.

Supplementary Figure 9. Cycling performance of LFP half cells with liquid electrolyte as cathode interlayer at RT and 45 °C.

Supplementary Figure 10. Cycling performance of Li||LFMP cell with molten salts as catholyte at 45 °C.

a

b

c

d

Supplementary Figure 11. Finite element analysis of Model 1 with low σ and DLi+ and Model 2 with high σ and DLi+ during the discharge process. a The built model for simulation. b The EIS spectra of Li||LFP half cells modified by molten salts and PEO-LiTFSI. c The ion diffusion coefficient fitted by EIS. d The Voltage-Time plot for Model 1 (PEO-LiTFSI) and Model 2 (molten salts) through simulation.

| Battery structure | Temperature (°C) | Cathode Fabrication | Mass loading (mg cm-2) | Rate/ current | Voltage (V vs Li/Li+) | Cycling number | Ref. in main text |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Li-SnF2/LLZO/liquid electrolyte/LFP | 30 | Slurry coating | ~1.6 ~3.3 | 0.5 C 1 C 0.2 C | 2.5–4.0 | 200 200 90 | 42 |
| Li-Ge/LLZO/PVDF-HFP &liquid electrolyte /LFP | RT | Slurry coating | ~0.6 | 1 C | 2.4–4.0 | 100 | 43 |
| Li/PEO-LiTFSI/LLZO/ PEO-LiTFSI /LFP | 90 | Slurry coating | ~2 | 0.2 C | 2.5–4.2 | 200 | 44 |
| Li/CPMEA-LiTFSI/LLZO/ CPMEA-LiTFSI /LFP | 65 | Slurry coating | ~5 | 0.2 C | 2.8–3.8 | 100 | 45 |
| Li /3D LLZO-ZnO/ LiTFSI- LFP | 60 | Slurry infiltration | ~2 | 0.2 C | 2.8–3.8 | 300 | 46 |
| Li/PVDF-HFP&LLZO&LiTFSI&TEGDME/LFP | 25 | Slurry coating | 2.1~2.3 | 0.5 C | 3.0–3.8 | 180 | 47 |
| Li/PVDF-PEO&LLZO NPs&LiTFSI/LFP | 50 | Slurry coating | ~1.5 | 0.2 C | 2.5–4.0 | 180 | 48 |
| Li/PEO-LiTFSI-LLZO NWs /LFP | 45 60 | Slurry coating | ~1.68 | 0.1 C 0.5 C | 2.8–4.2 | 80 70 | 49 |
| Li/PEO-LiTFSI & LLZO nanosheets | 45 60 | Slurry coating | ~1.2 | 0.3 C 0.5 C | 2.5–4.0 | 150 200 | 50 |
| Li/LLZTO/molten salts/LFP | 45 60 80 | Slurry coating | 3.3~3.8 | 0.5 C 0.5/1 C 0.5 C | 2.5–4.0 | 200 600/1000 200 | Our work |
|  | 100 |  |  | 2 C | 2.8–4.0 | 200 |  |
|  | 60 80 |  | ~12 | 0.1 C 0,2 C | 2.5–4.0 | 100 |  |
| Li/LLZTO/molten salts/LFMP | 45 |  | 3.1 | 0.5 C | 2.5–4.5 | 100 |  |
|  | 60 |  | 3.1 |  |  |  |  |

Table 1. Performance comparison with various strategies in garnet-type solid batteries

Reference

1.	Kubota, K.; Nohira, T.; Hagiwara, R., New inorganic ionic liquids possessing low melting temperatures and wide electrochemical windows: Ternary mixtures of alkali bis(fluorosulfonyl)amides. Electrochim. Acta 2012, 66, 320-324.