Supplementary Information

Re-valorization of Electronic Waste - Moss as a Biosorber for Gold Recovery?

Anna Maria Becker 1*, Benedikt Böhm 1, Christos Karampatzis 1, Patrik Blenk 1, Esther Gabor 2, Kathrin Castiglione 1

1Institute of Bioprocess Engineering, Friedrich-Alexander-Universität Erlangen-Nürnberg, Erlangen, Germany

2BRAIN Biotech AG, Zwingenberg, Germany

Corresponding author:

*Dr. Anna Maria Becker

Address:

Institute of Bioprocess Engineering

Department of Chemical and Biological Engineering

Friedrich-Alexander-Universität Erlangen-Nürnberg

Paul-Gordan-Straße 3

91052 Erlangen

Phone/Fax: +49 9131 8523185 / +49 9131 8523002

E-mail: anna.maria.becker@fau.de

ORCID: 0000-0001-6201-7770

Table A. Heating protocol for gold measurement using GF-AAS

| Phase | Temperature in °C | Ramp time in s | Hold time in s |
| --- | --- | --- | --- |
| 1 | 110 | 1 | 20 |
| 2 | 130 | 1 | 5 |
| 3 | 800 | 10 | 20 |
| 4 (Extinction measurement) | 1800 | 0 | 7 |
| 5 (Backing-out) | 2450 | 1 | 3 |

Table B. Gold sorption capacities and removal determined in single-component metal solutions

The dried biomass (BMd) of P. patens, P. eurystomum and P. sphaericum was weighed into separate vials, incubated for 24 h (RT) with 2 – 3 mL 10 mM solution of HAuCl4 (pH = 5) and the concentration of gold in the supernatant (Auend) was determined via AAS measurement (n = 3 for each sample) after centrifugation (10 min, 10,000 g, RT). Sorption capacities for gold (QAu) were calculated based on equation 1. Mean sorption capacities marked with an asterisk are significantly different from each other (two-sided, independent sample t-test (Excel), p* < 0.05).

| Species | BMd in mg | Auend in mM | ΔAu in µmol | QAu in mmol g-1 | Au removal in % | Mean QAu in mmol g-1 | Mean Au removal in % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| P. patens | 7 | 3.7 | 11.3 | 1.61 | 56 |  |  |
|  | 7.7 | 3.5 | 11.5 | 1.49 | 57 |  |  |
|  | 8.2 | 3.1 | 12.6 | 1.54 | 63 |  |  |
|  | 17.4 | 3.8 | 17.9 | 1.03 | 60 |  |  |
|  | 24.2 | 3.0 | 20.4 | 0.84 | 68 |  |  |
|  | 33.1 | 2.1 | 23.2 | 0.70 | 77 | 1.2 ± 0.4* | 64 ± 7 |
| P. eurystomum | 6.4 | 3.5 | 12.5 | 1.96 | 63 |  |  |
|  | 8.3 | 3.7 | 12.1 | 1.46 | 61 |  |  |
|  | 9.7 | 3.6 | 12.1 | 1.24 | 60 |  |  |
|  | 16.8 | 5.0 | 13.1 | 0.78 | 44 |  |  |
|  | 26.7 | 4.2 | 16.6 | 0.62 | 55 |  |  |
|  | 34.5 | 3.6 | 18.5 | 0.54 | 62 | 1.1 ± 0.5 | 57 ± 7 |
| P. sphaericum | 7.9 | 6.2 | 7.3 | 0.93 | 37 |  |  |
|  | 8.0 | 6.1 | 7.3 | 0.92 | 37 |  |  |
|  | 10.8 | 6.2 | 7.2 | 0.67 | 36 |  |  |
|  | 13.0 | 6.4 | 10.2 | 0.79 | 34 |  |  |
|  | 20.7 | 4.4 | 16.1 | 0.78 | 54 |  |  |
|  | 28.8 | 2.0 | 23.7 | 0.82 | 79 | 0.8 ± 0.1* | 46 ± 16 |

Table C. Terbium sorption capacities and removal determined in single-component metal solutions

The dried biomass (BMd) of P. patens, P. eurystomum and P. sphaericum was weighed into separate vials, incubated for 24 h (RT) with 2 mL 10 mM solution of Tb(NO3)3 (pH = 5) and the concentration of terbium in the supernatant (Tbend) was determined via XO Assay (n = 3 for each sample) after centrifugation (10 min, 10,000 g, RT). Sorption capacities for terbium (QTb) were calculated based on equation 1. Sorption capacities obtained for two respective moss species were analyzed using two-sided, independent sample t-test (Excel). Mean sorption capacities of P. patens were significantly different from those obtained for P. eurystomum and P. sphaericum (two-sided, independent sample t-test (Excel), ***p < 0.001).

| Species | BMd in mg | Tbend in mM | ΔTb in µmol | QTb in mmol g-1 | Tb removal in % | Mean QTb in mmol g-1 | Mean Tb removal in % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| P. patens | 10.1 | 10.3 | 4.9 | 0.49 | 25 |  |  |
|  | 22.7 | 7 | 11.6 | 0.51 | 58 |  |  |
|  | 25.9 | 3 | 13.4 | 0.52 | 67 |  |  |
|  | 29.4 | 2 | 15.6 | 0.53 | 78 |  |  |
|  | 33.0 | 4.3 | 17.1 | 0.52 | 86 |  |  |
|  | 40.7 | 1.7 | 16 | 0.39 | 80 | 0.49 ± 0.05 | 66 ± 20 |
| P. eurystomum | 13.7 | 10.8 | 3.6 | 0.26 | 18 |  |  |
|  | 23.7 | 8 | 9.3 | 0.39 | 47 |  |  |
|  | 25.6 | 3.7 | 10.6 | 0.41 | 53 |  |  |
|  | 36.7 | 2.6 | 13 | 0.35 | 65 |  |  |
|  | 36.8 | 5.9 | 13.3 | 0.36 | 67 |  |  |
|  | 40.6 | 2.3 | 13.6 | 0.33 | 68 | 0.35 ± 0.05 | 53 ± 17 |
| P. sphaericum | 11.8 | 10.8 | 3.7 | 0.31 | 19 |  |  |
|  | 22.1 | 5.9 | 7.5 | 0.34 | 38 |  |  |
|  | 25.0 | 5.1 | 8.6 | 0.34 | 43 |  |  |
|  | 25.1 | 8.6 | 7.5 | 0.30 | 38 |  |  |
|  | 27.2 | 5.5 | 8.2 | 0.30 | 41 |  |  |
|  | 28.7 | 8.3 | 8.2 | 0.29 | 41 | 0.31 ± 0.02 | 36 ± 8 |

Table D. Neodymium sorption capacities and removal determined in single-component metal solutions

The dried biomass (BMd) of P. patens, P. eurystomum and P. sphaericum was weighed into separate vials, incubated for 24 h (RT) with 2 mL 10 mM solution of Nd(NO3)3 (pH = 5) and the concentration of gold in the supernatant (Ndend) was determined via XO Assay (n = 3 for each sample) after centrifugation (10 min, 10,000 g, RT). Sorption capacities for neodymium (QNd) were calculated based on equation 1. The mean sorption capacities determined for all three moss species are not significantly different from each other (two-sided, independent sample t-tests (Excel), p > 0.05).

| Species | BMd in mg | Ndend in mM | ΔNd in µmol | QNd in mmol g-1 | Nd removal in % | Mean QNd in mmol g-1 | Mean Nd removal in % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| P. patens | 19.2 | 4.6 | 9.5 | 0.49 | 48 |  |  |
|  | 24.2 | 2.8 | 13.5 | 0.56 | 68 |  |  |
|  | 30.0 | 4.7 | 7.0 | 0.23 | 35 |  |  |
|  | 30.5 | 2.3 | 14.5 | 0.48 | 73 |  |  |
|  | 38.3 | 4.5 | 8.2 | 0.21 | 41 |  |  |
|  | 45.7 | 3.2 | 10.3 | 0.23 | 52 | 0.37 ± 0.14 | 53 ± 13 |
| P. eurystomum | 13.4 | 6.9 | 5.2 | 0.39 | 26 |  |  |
|  | 22.3 | 5.8 | 5.8 | 0.26 | 29 |  |  |
|  | 25.2 | 4.7 | 9.6 | 0.38 | 48 |  |  |
|  | 27.0 | 6.2 | 5.8 | 0.21 | 29 |  |  |
|  | 34.7 | 3.3 | 12.3 | 0.35 | 62 |  |  |
|  | 43.3 | 4.3 | 9.1 | 0.21 | 46 | 0.30 ± 0.08 | 40 ± 13 |
| P. sphaericum | 14.4 | 7.3 | 4.8 | 0.33 | 24 |  |  |
|  | 16.0 | 7.4 | 4.0 | 0.25 | 20 |  |  |
|  | 34.7 | 6.1 | 6.1 | 0.18 | 31 |  |  |
|  | 36.7 | 3.6 | 11.7 | 0.32 | 59 |  |  |
|  | 44.7 | 3.2 | 12.8 | 0.29 | 64 |  |  |
|  | 60.3 | 2.7 | 12.4 | 0.21 | 62 | 0.26 ± 0.06 | 43 ± 19 |

Table E. Sorption capacities and removal determined in two-component metal solutions of gold and terbium

The dried biomass (BMd) of P. patens, P. eurystomum and P. sphaericum was weighed into separate vials, incubated for 24 h (RT) with 2 mL of 5 mM solution (pH = 5) of each HAuCl4 and Tb(NO3)3 and the concentration of metal ions in the supernatant was determined either via XO Assay (Tb) or AAS (Au) (n = 3 for each sample) after centrifugation (10 min, 10,000 g, RT). Sorption capacities were calculated based on equation 1 and removal based on the initial and final concentration of the respective metal ions. The mean sorption capacities determined for all three moss species are not significantly different from each other (two-sided, independent sample t-tests (Excel), p > 0.05).

| Species | BMd in mg | Auend in mM | ΔAu in µmol | QAu in mmol g-1 | Au removal in % | Mean QAu / Removal Au | Tbend in mM | ΔTb in µmol | QTb in mmol g-1 | Tb removal in % | Mean QTb / Removal Tb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P. patens | 9.3 | 0.10 | 9.8 | 1.05 | 98 |  | 5.0 | 3.5 | 0.38 | 35 |  |
|  | 10.3 | 0.60 | 8.7 | 0.84 | 87 |  | 0.9 | 8.1 | 0.79 | 81 |  |
|  | 12.1 | 0.10 | 9.8 | 0.81 | 98 |  | 4.6 | 4.2 | 0.35 | 42 |  |
|  | 17.7 | 0.02 | 10.0 | 0.56 | 100 |  | 4.1 | 5.3 | 0.30 | 53 |  |
|  | 22.3 | 0.20 | 9.6 | 0.43 | 96 | 0.67 ± 0.26 / | 0.1 | 9.8 | 0.44 | 98 | 0.42 ± 0.17 / |
|  | 34.3 | 0.01 | 9.9 | 0.29 | 99 | 96 ± 4 | 0.1 | 9.8 | 0.29 | 98 | 68 ± 26 |
| P. eurystomum | 7.4 | 0.6 | 8.7 | 1.18 | 87 |  | 5.0 | 3.0 | 0.41 | 30 |  |
|  | 14.0 | 0.01 | 10.0 | 0.71 | 100 |  | 3.6 | 5.7 | 0.41 | 57 |  |
|  | 14.1 | 1.40 | 7.0 | 0.50 | 70 |  | 2.4 | 4.9 | 0.35 | 49 |  |
|  | 20.5 | 0.04 | 9.9 | 0.48 | 99 |  | 4.7 | 2.7 | 0.13 | 27 |  |
|  | 27.5 | 0.30 | 9.3 | 0.34 | 93 | 0.58 ± 0.30 / | 0.4 | 9.1 | 0.33 | 91 | 0.32 ± 0.09 / |
|  | 34.1 | 0.03 | 9.9 | 0.29 | 99 | 91 ± 11 | 0.1 | 9.8 | 0.29 | 98 | 59 ± 27 |
| P. sphaericum | 7.4 | 1.50 | 6.9 | 0.93 | 69 |  | 5.6 | 2.4 | 0.32 | 24 |  |
|  | 13.5 | 0.30 | 9.3 | 0.69 | 93 |  | 2.0 | 5.7 | 0.42 | 57 |  |
|  | 14.4 | 0.03 | 9.9 | 0.69 | 99 |  | 5.3 | 2.6 | 0.18 | 26 |  |
|  | 21.8 | 0.01 | 10.0 | 0.46 | 100 |  | 4.4 | 4.1 | 0.19 | 41 |  |
|  | 28.2 | 0.01 | 9.9 | 0.35 | 99 | 0.56 ± 0.23 / | 0.5 | 8.9 | 0.32 | 89 | 0.28 ± 0.08 / |
|  | 38.8 | 0.01 | 9.9 | 0.26 | 99 | 93 ± 11 | 0.1 | 9.8 | 0.25 | 98 | 56 ± 29 |

Table F. Sorption capacities and removal determined in two-component metal solutions of gold and neodymium

The dried biomass (BMd) of P. patens, P. eurystomum and P. sphaericum was weighed into separate vials, incubated for 24 h (RT) with 2 mL of 5 mM solution (pH = 5) of each HAuCl4 and Nd(NO3)3, and the concentration of metal ions in the supernatant was determined either via XO Assay (Nd) or AAS (Au) (n = 3 for each sample) after centrifugation (10 min, 10,000 g, RT). Sorption capacities were calculated based on equation 1 and removal based on the initial and final (Auend) concentration of the respective metal ions. The mean sorption capacities determined for all three moss species are not significantly different from each other (two-sided, independent sample t-tests (Excel), p > 0.05).

| Species | BMd in mg | Auend in mM | ΔAu in µmol | QAu in mmol g-1 | Au removal in % | Mean QAu / Removal Au | Ndend in mM | ΔNd in µmol | QNd in mmol g-1 | Nd removal in % | Mean QNd / Removal Nd |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P. patens | 8.1 | 0.40 | 9.2 | 1.14 | 92 |  | 2.0 | 5.9 | 0.73 | 35 |  |
|  | 13.8 | 0.10 | 9.8 | 0.71 | 98 |  | 1.8 | 6.2 | 0.45 | 42 |  |
|  | 15.6 | 1.0 | 7.9 | 0.51 | 79 |  | 2.0 | 5.8 | 0.37 | 81 |  |
|  | 20.6 | 0.03 | 9.9 | 0.48 | 99 |  | 1.4 | 7.1 | 0.34 | 53 |  |
|  | 23.9 | 0.2 | 9.6 | 0.40 | 96 | 0.59 ± 0.27 / | 0.2 | 9.6 | 0.40 | 98 | 0.43 ± 0.14 / |
|  | 31.1 | 0.01 | 9.9 | 0.32 | 99 | 94 ± 7 | 0.1 | 9.8 | 0.31 | 98 | 74 ± 16 |
| P. eurystomum | 8.3 | 0.7 | 8.5 | 1.02 | 85 |  | 3.9 | 1.7 | 0.21 | 30 |  |
|  | 13.4 | 2.0 | 5.7 | 0.43 | 57 |  | 2.7 | 4.2 | 0.31 | 91 |  |
|  | 16.9 | 0.1 | 9.8 | 0.58 | 98 |  | 1.9 | 5.6 | 0.33 | 57 |  |
|  | 20.0 | 1.1 | 7.5 | 0.38 | 75 |  | 2.0 | 5.5 | 0.28 | 98 |  |
|  | 30.3 | 0.6 | 8.7 | 0.29 | 87 | 0.49 ± 0.26 / | 1.0 | 7.8 | 0.26 | 49 | 0.26 ± 0.06 / |
|  | 39.1 | n.d. | 10 | 0.26 | >99 | 84 ± 15 | 1.4 | 6.4 | 0.16 | 27 | 52 ± 19 |
| P. sphaericum | 8.5 | 1.7 | 6.5 | 0.76 | 65 |  | 2.4 | 5 | 0.59 | 24 |  |
|  | 11.8 | 2.1 | 5.3 | 0.45 | 53 |  | 2.0 | 5.5 | 0.47 | 98 |  |
|  | 16.4 | 0.2 | 9.6 | 0.59 | 96 |  | 2.2 | 5.3 | 0.32 | 26 |  |
|  | 23.8 | n.d. | 10 | 0.42 | >99 |  | 1.9 | 5.9 | 0.25 | 41 |  |
|  | 26.5 | 0.1 | 9.8 | 0.37 | 98 | 0.48 ± 0.15 / | 2.0 | 5.7 | 0.21 | 57 | 0.36 ± 0.13 / |
|  | 32.5 | 0.01 | 9.9 | 0.30 | 99 | 85 ± 19 | 0.2 | 9.5 | 0.29 | 89 | 61 ± 15 |

n.d. < limit of detection (LOD) = 0.03 µM

Table G. Gold sorption capacities by P. patens at different pH

The dried biomass (10 – 20 mg) of P. patens was incubated for 24 h (RT) with 3 mL 10 mM solution of HAuCl4 with different pH (3 to 9.2) (n = 6). The pH of solution was adjusted by addition of NaOH/HCl. The final concentration of gold in the supernatant (Auend) was determined via AAS measurement (n = 3) for each sample after centrifugation (10 min, 10,000 g, RT) and the final pH (pHend) of the supernatant measured again at the end of the incubation. Sorption capacities for gold (QAu) were calculated based on equation 1. The mean sorption capacity obtained for the solution with pH 6 was significantly different from the values recorded for solutions with pH 4 and 5 (two-sided, independent sample t-test (Excel), p < 0.001. Other pairs were not analyzed.

| pH | BMd in mg | Auend in mM | ΔAu in µmol | QAu in mmol g-1 | pHend | Mean QAu in mmol g-1 | Mean pHend |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 3 | 10.8 | 8.88 | 4.52 | 0.42 | 2.48 |  |  |
|  | 9.0 | 9.90 | 1.62 | 0.18 | 2.59 |  |  |
|  | 9.1 | 10.6 | - | 0 | 2.60 |  |  |
|  | 20.0 | 6.28 | 12.36 | 0.62 | 2.24 |  |  |
|  | 19.3 | 5.89 | 12.72 | 0.66 | 2.25 |  |  |
|  | 19.6 | 7.03 | 9.93 | 0.51 | 2.23 | 0.40 ± 0.24 | 2.4 ± 0.2 |
| 4 | 9.8 | 7.57 | 6.5 | 0.66 | 2.98 |  |  |
|  | 9.4 | 6.3 | 10.51 | 1.12 | 2.93 |  |  |
|  | 10.3 | 7.44 | 6.59 | 0.64 | 2.74 |  |  |
|  | 19.6 | 4.21 | 16.52 | 0.84 | 2.29 |  |  |
|  | 20.6 | 3.11 | 19.96 | 0.97 | 2.28 |  |  |
|  | 20.1 | 4.75 | 14.57 | 0.72 | 2.27 | 0.83 ± 0.17 | 2.6 ± 0.3 |
| 5 | 10.3 | 6.8 | 8.61 | 0.84 | 5.40 |  |  |
|  | 9.9 | 7.15 | 7.42 | 0.75 | 5.35 |  |  |
|  | 9.8 | 6.89 | 8.18 | 0.83 | 5.30 |  |  |
|  | 20.5 | 3.48 | 18.39 | 0.9 | 4.94 |  |  |
|  | 19.8 | 4.02 | 16.45 | 0.83 | 4.95 |  |  |
|  | 19.9 | 3.9 | 16.72 | 0.84 | 4.85 | 0.83 ± 0.05 | 5.1 ± 0.2 |
| 6 | 9.9 | 5.91 | 12.02 | 1.21 | 5.51 |  |  |
|  | 10.6 | 5.34 | 13.62 | 1.28 | 5.31 |  |  |
|  | 9.9 | 6.11 | 11.43 | 1.15 | 5.44 |  |  |
|  | 20.1 | 3.23 | 25.17 | 1.25 | 4.52 |  |  |
|  | 19.9 | 3.15 | 25.36 | 1.27 | 4.50 |  |  |
|  | 20.9 | 2.83 | 26.49 | 1.27 | 4.37 | 1.24 ± 0.05 | 4.9 ± 0.5 |
| 7 | 10.8 | 8.22 | 3.46 | 0.32 | 6.71 |  |  |
|  | 10.2 | 7.77 | 4.86 | 0.48 | 6.83 |  |  |
|  | 10.3 | 7.68 | 4.69 | 0.46 | 6.97 |  |  |
|  | 20.2 | 6.91 | 6.89 | 0.34 | 6.68 |  |  |
|  | 20.5 | 7.44 | 5.63 | 0.27 | 6.90 |  |  |
|  | 19.8 | 7.14 | 6.54 | 0.33 | 6.91 | 0.37 ± 0.08 | 6.8 ± 0.1 |
| 9.2 | 10.5 | 8.83 | 1.77 | 0.17 | 6.69 |  |  |
|  | 9.2 | 8.32 | 3.41 | 0.37 | 7.28 |  |  |
|  | 9.9 | 10.31 | - | 0 | 7.26 |  |  |
|  | 19.8 | 8.46 | 1.64 | 0.08 | 7.00 |  |  |
|  | 20 | 7.83 | 4.17 | 0.21 | 7.15 |  |  |
|  | 20.7 | 7.83 | 3.74 | 0.18 | 7.20 | 0.17 ± 0.11 | 7.1 ± 0.2 |

Figure A. Color change observed after the incubation of the biomass of P. patens in a gold solution.

Presented are the color changes in the supernatants after centrifugation (a.) and of the biomass (b.) observed after the incubation of the dried biomass of P. patens with 3 mL 10 mM solution of HAuCl4 (pH 6). Gold deposits inside the reaction tubes are clearly visible (c.)

Table H. Sorption capacities and removal of gold from biolechate of an industrial recycling material.

Mean sorption capacities (n = 6) obtained for the biomass of P. patens, P. eurystomum and P. sphaericum by incubation with bioleachate of e-waste. Dried biomass (10 - 40 mg) of the respective moss was incubated (room temperature, 24 h) with 3 mL of bioleachate solution (39.2 µM Au, pH adjusted with 1 M HCl to 5). Gold concentration after the incubation (Cf) was determined in the supernatant after centrifugation via ICP-MS and Q calculated according to equation 1. The mean sorption capacities determined for all three moss species are not significantly different from each other (two-sided, independent sample t-tests (Excel), p > 0.05).

| Species | BMd in mg | Auend in µM | ΔAu in nmol | QAu in µmol g-1 | Au removal in % | Mean QAu in µmol g-1 | Mean Au removal in % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| P. patens | 20.4 | 27.1 | 24.2 | 1.19 | 31 |  |  |
|  | 28.5 | 28.1 | 22.2 | 0.78 | 28 |  |  |
|  | 39.0 | 24.9 | 28.6 | 0.73 | 36 |  |  |
|  | 12.9 | 24.4 | 29.6 | 2.29 | 38 |  |  |
|  | 21.5 | 22.0 | 34.4 | 1.60 | 44 |  |  |
|  | 27.0 | 20.7 | 37.0 | 1.37 | 47 | 1.33 ± 0.53 | 37 ± 7 |
| P. eurystomum | 38.5 | 24.8 | 28.8 | 0.75 | 37 |  |  |
|  | 25.4 | 27.3 | 23.8 | 0.94 | 30 |  |  |
|  | 19.7 | 27.6 | 23.2 | 1.18 | 30 |  |  |
|  | 10.9 | 25.4 | 27.6 | 2.53 | 35 |  |  |
|  | 17.1 | 25.5 | 27.4 | 1.60 | 35 |  |  |
|  | 26.0 | 19.9 | 38.6 | 1.48 | 49 | 1.41 ± 0.58 | 36 ± 7 |
| P. sphaericum | 19.7 | 25.3 | 27.8 | 1.41 | 35 |  |  |
|  | 28.8 | 24.5 | 29.4 | 1.02 | 38 |  |  |
|  | 35.6 | 24.0 | 30.4 | 0.85 | 39 |  |  |
|  | 22.0 | 22.9 | 32.6 | 1.48 | 42 |  |  |
|  | 10.0 | 28.0 | 22.4 | 2.24 | 29 |  |  |
|  | 30.0 | 22.1 | 34.2 | 1.14 | 44 | 1.36 ± 0.45 | 38 ± 5 |