Supplementary material

Table S1 Pore parameters of different biochars

| Pyrolysis type |  | aSBET(m2/g) | bSmicro(m2/g) | cVtotal(cm3/g) | bVmicro(cm3/g) | dDaverage(nm) |
| --- | --- | --- | --- | --- | --- | --- |
| MP | MPB300 | 1.0338 | 0.8062 | 0.003407 | 0.000362 | 13.1831 |
|  | MPB400 | 1.9671 | 1.6304 | 0.004567 | 0.000756 | 10.2862 |
|  | MPB500 | 2.8826 | 1.7512 | 0.007881 | 0.000821 | 7.9360 |
|  | MPB600 | 3.9608 | 3.7516 | 0.008939 | 0.001796 | 5.2832 |
|  | MPB700 | 16.2748 | 13.7036 | 0.0093966 | 0.004976 | 1.5719 |
| EP | EPB300 | 0.8283 | 0.0395 | 0.005303 | 0.000004 | 25.6095 |
|  | EPB400 | 1.7075 | 0.7418 | 0.0047741 | 0.000336 | 11.1064 |
|  | EPB500 | 2.3236 | 1.7271 | 0.005011 | 0.000799 | 8.6264 |
|  | EPB600 | 3.7581 | 3.5681 | 0.006247 | 0.001692 | 6.6491 |
|  | EPB700 | 8.5603 | 8.3207 | 0.009087 | 0.003855 | 4.2464 |

a Brunauer, Emmett and Teller (BET) method.

b Determine by the t-plot method.

c Determine at relative pressure P/P0=0.99.

d Adsorption average pore diameter (4V/A by BET).

Table S2 Percentage of total C in aliphatic-C, aromatic-C, carboxyl-C, and carbonyl-C in cow manure biochar as determined by 13C NMR

| Chemical shift (ppm) |  | 0-90 | 90-160 | 160-245 |
| --- | --- | --- | --- | --- |
|  |  | aliphatic-C | aromatic-C | carboxyl-C and carbonyl-C |
| MP | MPB300 | 43.19 | 54.11 | 2.70 |
|  | MPB400 | 30.70 | 66.95 | 2.35 |
|  | MPB500 | 2.84 | 95.50 | 1.65 |
|  | MPB600 | 1.21 | 97.48 | 1.31 |
|  | MPB700 | 0.69 | 98.77 | 0.54 |
| EP | EPB300 | 44.24 | 50.33 | 5.44 |
|  | EPB400 | 31.76 | 64.61 | 3.63 |
|  | EPB500 | 10.74 | 86.30 | 2.96 |
|  | EPB600 | 2.53 | 95.57 | 1.90 |
|  | EPB700 | 1.26 | 97.67 | 1.07 |

Table S3 Basic properties of cow manure

| Ultimate analysis |  |  |  |  | Proximate analysis |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C(wt%)ad | H(wt%)ad | N(wt%)ad | S(wt%)ad | O(wt%) c | Mositure content(wt%) ar | Volatile matter(wt%)ad | Fixed carbon(wt%)ad | Ash(wt%)ad |
| 40.10±1.64 | 5.32±0.21 | 1.68±0.64 | 0.41±0.23 | 33.68±2.11 | 80.09±2.67 | 66.12±1.28 | 15.07±0.15 | 18.81±0.83 |

ar : as received basis      ad: air dry basis     c: O was calculated by difference