## Slide 1
Figure 10b
Chart: oxidation time, h
| 0 | 1 | 5 | 10 | 15 | 25 | 50 | 75 | 100 | 100 | 125 | 150 | 175 | 200 | 225 | 250 | 275 | 300 | 300 | 325 | 350 | 375 | 400 | 425 | 450 | 475 | 500
corrected 1300 C' | 0.30851 | 0.29685 | 0.40799 | 0.49642 | 0.56458 | 0.67388 | 0.88021 | 1.0098 | 1.1013 | 1.1013 | 1.1676 | 1.2388 | 1.3058 | 1.3764 | 1.42 | 1.4501 | 1.4955 | 1.5925 | 1.5925 | 1.6435 | 1.657 | 1.6969 | 1.7282 | 1.7657 | 1.8191 | 1.9131 | 1.945
Mach 0.3 data
cubic-linear fit
(b)

## Slide 2
Figure A1. One-to-one correspondence of kp estimated as Fp (ΔWmax)2/tmax (ordinate) with that determined from COSP model fits of target material tests (abscissa). Relations shown for exact stoichiometric factors, Fp, (squares, dashed blue line) and 4.06 average value (filled circles, solid green line); eqn. A8 and Table A1.

## Slide 3
Figure A2. One-to-one correspondence of kv estimated as Fv (ΔWmax)/tmax (ordinate) with that determined from COSP model fits of target material tests (abscissa). Relations shown for exact stoichiometric factors, Fv, (squares, solid blue line) and 1.16 average value (filled circles, dashed green line); eqn. A9 and Table A1.

## Slide 4
Figure B1
Figure B1. Comparisons for paralinear and COSP fits to replotted Tedmon1 Δw/A vs log t results for Cr-Cr2O3 oxidation at 1200 °C. COSP Model #3 is a better fit for most long-time data (>30-280 h). Model #4 (~ Tedmon curve) fits better for short times (1-10 h).
Solid black: Parabolic: kp = 0.54 mg2/cm4/h
Blue large circles: experimental data points
Teal small circles: data matched at Δw(max), Δw(final)
Blue long dash: matched Tedmon analytical curve, but using kv = Q0 /Δt = 0.048 mg/cm2/h
Red short dashed: using kv = Qo /Δt = 0.058 mg/cm2/h from Hagel.19
Cr-0.2Y (Cr2O3)
Paralinear Behavior
(Tedmon)
4
2
1
5
3
1 h
10 h
100 h