| Table 6: Comparison between the results of porous medium-based experimental studies |  |  |  |  |
| --- | --- | --- | --- | --- |
| No. | Reference | Temperature reduction | Remarks | Image |
| 1 | Hasan andFarhan (2019) | 5.25 ˚C | Irradiance: 950 W/m2 Air flow: 3.6 m/s Ambient temperature: 28 °C Fin: 10 longitudinal copper porous media |  |
| 2 | Kim et al. (2020) | 1.49 °C | Irradiance: 1000 W/m2 Air flow: 0.5 m/s Ambient temperature: 25 °C Heat sink: metallic mesh |  |
| 3 | Hasan andFarhan (2020) | 3˚C | Irradiance: 1050 W/m2 Air flow: 4 m/s Ambient temperature: 39 °C Fin: Copper porous media |  |
| 4 | Selimefendigil et al. (2018) | 1.5 ˚C | Irradiance (max): 906 W/m2 Air flow (average): 2.7 m/s Ambient temperature: 24 °C Fin: Aluminum foam |  |
| 5 | Shastry andArunachala (2020) | 4.5˚C | Irradiance: 800 W/m2 Air flow: 0 m/s Ambient temperature: not mentioned Fin: Aluminum mesh |  |
| 6 | Essa et al. (2021) | 9.5 ˚C | Irradiance: 900 W/m2 Air flow: 0 m/s Ambient temperature: not mentioned Heat sink: Copper porous medium + PCM |  |
| 7 | Firoozzadeh andShiravi (2022) | 21.5 ˚C | Irradiance: 630 W/m2 Air flow: 0 m/s Ambient temperature: 35 °C Heat sink: Aluminum porous medium + PCM |  |
| 8 | Vaziri Rad et al. (2021) | 24 ˚C | Irradiance: 997 W/m2 Air flow: 0.5 m/s Ambient temperature: 25 °C Heat sink: Aluminum shaving + PCM + water circulation |  |
| 9 | The present study | 18.3 ˚C | Irradiance: 630 W/m2 Air flow: 0.56 m/s (2 km/h) Ambient temperature: 35 °C Heat sink: Aluminum porous medium |  |