Supporting Information

CuFe2O4@SiO2@l-arginine@Cu(I) as a new magnetically retrievable heterogeneous nanocatalyst with high efficiency for triazole synthesis

Fatemeh Salehzadeh1, Maryam Esmkhani1, Mahsa Zallaghi1, Shahrzad Javanshir1*, Mohammad G. Dekamin1

1 Pharmaceutical and Heterocyclic Compounds Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran, 16846-13114, Iran

Figure S 1. FT-IR spectra of the a) CuFe2O4, b) CuFe2O4@SiO2, and c) CuFe2O4@SiO2@arginine@Cu(I).	2

Figure S 2. VSM analysis of CuFe2O4, CuFe2O4@SiO2 and CuFe2O4@SiO2@l-arginine@Cu (I).	2

Figure S 3. XRD pattern of: a) CuFe2O4, b) CuFe2O4@SiO2, c) CuFe2O4@SiO2@l-arginine@Cu (I).	3

Figure S 4. Recyclability of CuFe2O4@SiO2@l-arginine@Cu(I).	3

Table S 1. Investigation of the prepared catalyst in different conditions in model reaction.	3

Table S 2. Optimization of the type of catalyst.	4

Figure S 1. FT-IR spectra of the a) CuFe2O4, b) CuFe2O4@SiO2, and c) CuFe2O4@SiO2@arginine@Cu(I).

Figure S 2. VSM analysis of CuFe2O4, CuFe2O4@SiO2 and CuFe2O4@SiO2@l-arginine@Cu (I).

Figure S 3. XRD pattern of: a) CuFe2O4, b) CuFe2O4@SiO2, c) CuFe2O4@SiO2@l-arginine@Cu (I).

Figure S 4. Recyclability of CuFe2O4@SiO2@l-arginine@Cu(I).

Table S 1. Investigation of the prepared catalyst in different conditions in model reaction.

| Entry | Solvent | Catalyst (mg) | Condition | Time (min) | Yield % |
| --- | --- | --- | --- | --- | --- |
| 1 | H2O | 10 | Reflux | 45 | 52 |
| 2 | EtOH | 10 | Reflux | 45 | 42 |
| 3 | H2O:EtOH(1:1) | 10 | Reflux | 45 | 35 |
| 4 | Toluene | 10 | Reflux | 45 | Trace |
| 5 | H2O | 10 | Ultrasonic | 25 | 55 |
| 6 | EtOH | 10 | Ultrasonic | 25 | 52 |
| 7 | Chloroform | 10 | Ultrasonic | 25 | 40 |
| 8 | MeCN | 10 | Ultrasonic | 25 | 45 |
| 9 | H2O:EtOH(1:1) | 10 | Ultrasonic | 25 | 65 |
| 10 | H2O:EtOH(1:2) | 10 | Ultrasonic | 25 | 60 |
| 011 | H2O:EtOH(1:1) | - | Ultrasonic | 25 | - |
| 12 | H2O:EtOH(1:1) | 5 | Ultrasonic | 25 | 69 |
| 13 | H2O:EtOH(1:1) | 10 | Ultrasonic | 25 | 65 |
| 14 | H2O:EtOH(1:1) | 15 | Ultrasonic | 25 | 87 |
| 15 | H2O:EtOH(1:1) | 20 | Ultrasonic | 25 | 79 |
| 16 | H2O:EtOH(1:1) | 30 | Ultrasonic | 25 | 89 |

Table S 2. Optimization of the type of catalyst.

| Entry | Catalyst (15 mg) | Time (min) | Yield % |
| --- | --- | --- | --- |
| 1 | CuFe2O4 | 25 | 73 |
| 2 | CuFe2O4@SiO2 | 25 | 65 |
| 3 | CuFe2O4@SiO2@l-arginine | 25 | 68 |
| 4 | CuFe2O4@SiO2@l-arginine-Cu(I) | 25 | 87 |