Supplementary Information

Operando reconstruction towards CuI nanodots with favorable facets and stable Cu+ state for selective CO2-to-C2H4 conversion

Wenjie Xue1, Hongxia Liu2, Ruoou Yang3, Youwen Liu3, Bao Yu Xia1 and Bo You1*

1Key Laboratory of Material Chemistry for Energy Conversion and Storage, Ministry of education, Hubei Key Laboratory of Material Chemistry and Service Failure, School of Chemistry and Chemical Engineering, Huazhong University of Science and Technology, Wuhan, Hubei, 430074, China

2School of Chemistry and Chemical Engineering, Wuhan Textile University, Wuhan, 430200, China

3State Key Laboratory of Materials Processing and Die & Mould Technology, and School of Materials Science and Engineering Huazhong University of Science and Technology Wuhan, Hubei, 430074, China

*Corresponding author. Email: youbo@hust.edu.cn

- Supplementary data

Supplementary Fig. 1 XRD pattern of the Cu(OH)2 precursors.

Supplementary Fig. 2 High-resolution Cu 2p XPS spectra of CuI-CO2, CuI-N2 and Cu-CO2 catalysts.

Supplementary Fig. 3 SEM image of the CuI-CO2 catalysts.

Supplementary Fig. 4 a TEM and b HR-TEM image of Cu(OH)2 precursors.

Supplementary Fig. 5 The main product distributions in CO2-saturated 0.1 M KHCO3/KI solution during the synthesis of CuI-CO2 catalysts.

Supplementary Fig. 6 Standard curves for the main liquid products of a formate and b ethanol using 1H NMR analysis.

Supplementary Fig. 7 a Current density vs potential curves of CuI-CO2, CuI-N2 and Cu-CO2 catalysts for CO2 electroreduction. b Nyquist plots of CuI-CO2, CuI-N2 and Cu-CO2 catalysts. Electrochemical impedance spectrums uncover a similar contact resistance between CuI-CO2 (26.09 ohm) and CuI-N2 (26.25 ohm), and a slight lower contact resistance for Cu-CO2 (21.65 ohm) as indicated by the approximate equivalent series resistance (ESR) obtained from the x-intercept of the Nyquist plots.

Supplementary Fig. 8 Cyclic voltammograms of a CuI-CO2. b CuI-N2 and c Cu-CO2 catalysts at scan rates from 5 to 50 mV s-1. d Scan rate dependence of the current densities of CuI-CO2, CuI-N2 and Cu-CO2 catalysts for ECSA measurements.

Supplementary Fig. 9 TEM images of a CuI-N2 and b Cu-CO2 catalysts.

Supplementary Fig. 10 High-resolution XPS spectra for a Cu 2p and b I 3d of CuI-CO2 catalysts after 20 h stability test in a H-cell.

Supplementary Fig. 11 a XRD pattern, b TEM image and c HR-TEM image of CuI-CO2 electrocatalysts after 12 h stability test at 400 mA cm-2 in a flow cell.

Supplementary Fig. 12 Crystal face models of a Cu(111) for Cu-CO2 catalysts. b CuI(111). c CuI(220). d CuI(311) for CuI-CO2 catalysts.

Supplementary Table 1 FEs of CuI-CO2 for CO2R at different potentials in a H-cell.

| Potential (V) | FE (%) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | C2H4 | C2H5OH | C2H6 | CH4 | CO | HCOOH | H2 |
| -0.9 | 22.6 | 0.0 | 0.0 | 0.0 | 26.4 | 19.1 | 28.0 |
| -1 | 31.7 | 6.5 | 0.2 | 0.6 | 14.6 | 14.5 | 31.2 |
| -1.1 | 40.1 | 12.7 | 0.3 | 1.1 | 7.4 | 9.0 | 28.3 |
| -1.2 | 45.3 | 13.3 | 0.0 | 1.3 | 11.7 | 5.4 | 21.5 |
| -1.3 | 42.2 | 9.7 | 0.0 | 4.3 | 8.3 | 3.1 | 33.0 |
| -1.4 | 32.3 | 3.3 | 0.2 | 7.8 | 3.0 | 2.8 | 51.4 |

| Potential (V) | FE (%) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | C2H4 | C2H5OH | C2H6 | CH4 | CO | HCOOH | H2 |
| -0.9 | 14.5 | 0 | 0.0 | 0.0 | 21.9 | 11.2 | 52.6 |
| -1 | 21.4 | 0.0 | 0.0 | 0.2 | 15.2 | 10.7 | 51.5 |
| -1.1 | 30.6 | 3.1 | 0.0 | 1.0 | 9.3 | 9.2 | 45.2 |
| -1.2 | 35.7 | 8.3 | 0.0 | 3.0 | 7.7 | 8.5 | 36.6 |
| -1.3 | 34.0 | 8.1 | 0.0 | 5.0 | 3.6 | 4.3 | 44.1 |
| -1.4 | 23.7 | 2.5 | 0.0 | 5.0 | 1.3 | 2.7 | 62.1 |

Supplementary Table 2 FEs of CuI-N2 for CO2R at different potentials in a H-cell.

Supplementary Table S3 FEs of Cu-CO2 for CO2R at different potentials in a H-cell.

| Potential (V) | FE (%) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | C2H4 | C2H5OH | C2H6 | CH4 | CO | HCOOH | H2 |
| -0.9 | 7.0 | 0.0 | 0.0 | 0.7 | 19.2 | 16.3 | 56.9 |
| -1 | 11.7 | 3.2 | 0.0 | 4.5 | 13.9 | 13.4 | 54.3 |
| -1.1 | 15.6 | 5.2 | 0.0 | 0.9 | 10.4 | 11.8 | 51.7 |
| -1.2 | 24.9 | 5.3 | 0.0 | 3.6 | 5.2 | 7.3 | 50.9 |
| -1.3 | 26.5 | 4.7 | 0.0 | 6.4 | 4.9 | 4.2 | 49.0 |
| -1.4 | 20.4 | 2.4 | 0.0 | 7.2 | 3.9 | 3.7 | 62.6 |

| Current density (mA cm-2) | FE (%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | C2H4 | CH4 | CO | H2 |
| 400 | 47.6 | 0.65 | 28.24 | 16.7 |
| 500 | 56.98 | 4.51 | 14.92 | 13.27 |
| 600 | 59.85 | 0.9 | 16.19 | 17.97 |
| 700 | 71.85 | 3.64 | 18.35 | 12.23 |
| 800 | 72.43 | 6.42 | 11.39 | 13.27 |
| 900 | 65.5 | 7.22 | 8.23 | 24.97 |
| 1000 | 55.12 | 8.46 | 5.37 | 41.98 |

Supplementary Table 4 FEs of CuI-CO2 for CO2R at different potentials in a flow cell.

Supplementary Table 5 Comparison of CO2R performance of CuI-CO2 with recently reported Cu-based catalysts in a flow cell.

| Materials | J (mA cm-2) | FE of C2H4 | Electrolyte | Reference |  |
| --- | --- | --- | --- | --- | --- |
| CuI-CO2 | 800 | 72.4% | 0.5 M KHCO3/KI | This work |  |
| S-HKUST-1 | 400 | 57% | 1.0 M KOH | Angew. Chem. Int. Ed. 61, e202111700 (2022). | 1 |
| Cu dimer distorted HKUST-1 | 260 | 45% | 1.0 M KOH | J. Am. Chem. Soc. 140, 11378-11386 (2018). | 2 |
| graphite/carbon NPs/Cu/PTFE | 275 | 66% | 10.0 M KOH | Science 360, 783-787 (2018). | 3 |
| CuAl-GDE | 400 | 80% | 1.0 M KOH | Nature 581, 178-183 (2020). | 4 |
| molecular tuned Cu catalyst | ~320 | 72% | 1.0 M KHCO3 | Nature 577, 509-51 (2020). | 5 |
| Cu-F | 800 | 65% | 2.5 M KOH | Nat. Catal. 3, 478-487 (2020). | 6 |
| Cu-polyamine hybrid | ~433 | 72% | 1 M KOH | Nat. Catal. 4, 20-27 (2021). | 7 |
| Cu(OH)2-D/CP | ~250 | 58% | 1 M KOH | Angew. Chem. Int. Ed. 60, 4879-4885 (2021). | 8 |
| multihollow Cu2O | ~250 | 38% | 2 M KOH | J. Am. Chem. Soc. 142, 6400-6408 (2020). | 9 |
| Cu-CuI | ~710 | 35% | 1 M KOH | Angew. Chem. Int. Ed. 60, 14329-14333 (2021). | 10 |
| 3D porous CuO | ~653 | 39% | 1 M KOH | Adv. Mater. 30, 1803111 (2018). | 11 |
| CuAg Alloy | ~300 | 60% | 1 M KOH | J. Am. Chem. Soc. 140, 5791-5797 (2018). | 12 |
| AEI-OD-Cu nanosheets | 800 | 62% | 1 M KOH | J. Am. Chem. Soc. 144, 10446-10454 (2022). | 13 |
| Cu-PTFE NNs | 300 | 45% | 1 M KOH | J. Am. Chem. Soc. 144, 3039-3049 (2022) | 14 |

Supplementary References

- Wen, C. F. et al. Highly ethylene‐selective electrocatalytic CO2 reduction enabled by isolated Cu-S motifs in Metal–Organic Framework Based Precatalysts. Angew. Chem. Int. Ed. 61, e202111700 (2022).

- Nam, D. H. et al. Metal-organic frameworks mediate Cu coordination for selective CO2 electroreduction. J. Am. Chem. Soc. 140, 11378-11386 (2018).

- Dinh, C. T. et al. CO2 electroreduction to ethylene via hydroxide-mediated copper catalysis at an abrupt interface. Science 360, 783-787 (2018).

4. Zhong, M. et al. Accelerated discovery of CO2 electrocatalysts using active machine learning. Nature 581, 178-183 (2020).

5. Li, F. et al. Molecular tuning of CO2-to-ethylene conversion. Nature 577, 509-513 (2020).

6. Ma, W. et al. Electrocatalytic reduction of CO2 to ethylene and ethanol through hydrogen-assisted C-C coupling over fluorine-modified copper. Nat. Catal. 3, 478-487 (2020).

7. Chen, X. et al. Electrochemical CO2-to-ethylene conversion on polyamine-incorporated Cu electrodes. Nat. Catal. 4, 20-27 (2021).

8. Zhong, D. et al. Coupling of Cu (100) and (110) facets promotes carbon dioxide conversion to hydrocarbons and alcohols. Angew. Chem. Int. Ed. 60, 4879-4885 (2021).

9. Yang, P. P. et al. Protecting copper oxidation state via intermediate confinement for selective CO2 electroreduction to C2+ Fuels. J. Am. Chem. Soc. 142, 6400-6408 (2020).

10. Li, H. et al. High‐rate CO2 electroreduction to C2+ products over a copper‐copper iodide catalyst. Angew. Chem. Int. Ed. 60, 14329-14333 (2021).

11. Lv J. J. et al. A highly porous copper electrocatalyst for carbon dioxide reduction, Adv. Mater. 30, 1803111 (2018).

12. Hoang, T. T. H. et al. Nanoporous copper-silver alloys by additive-controlled electrodeposition for the selective electroreduction of CO2 to ethylene and ethanol, J. Am. Chem. Soc. 140, 5791-5797 (2018).

13. Zhao, Y. et al. Industrial-current-density CO2-to-C2+ electroreduction by anti-swelling anion-exchange ionomer-modified oxide-derived Cu nanosheets. J. Am. Chem. Soc. 144, 10446-10454 (2022).

14. Yang, B. et al. Accelerating CO2 electroreduction to multicarbon products via synergistic electric-thermal field on copper nanoneedles. J. Am. Chem. Soc. 144, 3039-3049 (2022).