Supplementary Information

Construction of double grafted interfacial layer to improve thermal and mechanical properties of carbon fiber reinforced polyamide 6 composites

Bowen Lia, Guojun Songa,*, Zhi Penga,*, Wenjian Zhanga, Hao Zhenga, Junjie Zhua, Chaohang Wanga, Jianfa Wanga, Xiaoping Yanga, Ruiyue Maa, Shaoqian Zhua, Xiaoping Yangb, Yudong Huangb, Lichun Ma a,b,*

aInstitute of Polymer Materials, School of Material Science and Engineering, Qingdao University, Qingdao 266071, China

bState Key Laboratory of Organic-Inorganic Composites, Beijing University of Chemical Technology, Beijing, 100029, China

*Author to whom correspondence should be addressed. Electronic mail: malcqdu@163.com (L. Ma), songguojunqdu@126.com (G. Song)

Fig. S1 Schematic routes for fabrication process for CFs/PA6 composites.

Fig. S2 DMA results: (a) storage modulus and (b) tan delta of CFs/PA6 composites.

Table S1 The relative elemental composition and active groups of CFs.

| Samples | Element content (%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | C | N | O | Si |
| untreated CF | 87.59 | 1.88 | 10.53 | 0 |
| CF-PDA | 73.56 | 3.31 | 23.13 | 0 |
| CF-SiO2 | 81.60 | 1.04 | 14.28 | 3.08 |
| CF-PDA -SiO2 | 70.36 | 2.89 | 17.83 | 8.92 |

Table S2 Contact angles and surface energy of different CFs.

| Samples | Contact Angles (°) |  | Surface Energy (mN·m−1) |  |  |
| --- | --- | --- | --- | --- | --- |
|  | θwater | θdiiodomethane | γd | γp | γ |
| untreated CF | 88.38 | 54.01 | 32.11 | 2.39 | 34.5 |
| CF-PDA | 56.54 | 40.26 | 39.34 | 14.24 | 53.58 |
| CF-SiO2 | 65.94 | 47.68 | 35.42 | 10.86 | 46.28 |
| CF-PDA-SiO2 | 44.35 | 31.83 | 43.48 | 19.85 | 63.33 |