Simultaneous Adsorption of Chromium and Acidic Dye from Leather Tannery Model Wastewater Using a Novel Modified Nanoclay

Journal of Environmental Earth Sciences

M. Golghasemi Sorkhabia, H. Aghdasiniaa*, F. Notghi Oskuia, A, Karimib, M. Golizadehb

a Faculty of chemical and petroleum engineering, University of Tabriz, Tabriz, Iran

b Faculty of advanced technologies in medicine, Iran university of medical sciences, 1449614535 Tehran, Iran

* Corresponding author:		Hassan Aghdasinia

E-mail address: 			aghdasinia@tabrizu.ac.ir/ Hassan.Aghdasinia@gmail.com

Tel: +98-41-3339-2931		Fax: +98-41-3333-8497

E-mail addresses of authors:

Mahsa Golghasemi Sorkhabi		 Mahsa.Golghasemi@gmail.com

Fatemeh Notghi Oskui		               Notghi1992@gmail.com

Afzal Karimi				Karimi.af@iums.ac.ir

Mortaza Golizadeh			Mor.golizadeh@gmail.com

List of Figures:

1) Parity plot for (a) dye and (b) Cr (III).

2) The normal probability of the residuals for (a) dye and (b) Cr (III).

| (b) | (a) |
| --- | --- |
| Fig. 1 |  |

| (b) | (a) |
| --- | --- |
| Fig. 2 |  |

List of Tables:

1) Non-linear isotherm parameters for simultaneous adsorption of Cr (III).

2) Non-linear isotherm parameters for simultaneous adsorption of dye.

3) Non-linear isotherm parameters for single adsorption of Cr (III).

4) Non-linear isotherm parameters for single adsorption of dye.

5) Adsorption capacities for Langmuir isotherm.

6) RL values of Langmuir isotherm.

Table 1

| Langmuir isotherm |  |  |  |
| --- | --- | --- | --- |
| Error function |  |  |  |
| Chi square | HYBRID | SSE |  |
| 193.1401 | 193.1390 | 32.9671 | qmL |
| 0.3267 | 0.3269 | 3.0591 | b |
| 74.2864 | 74.2864 | 62.1031 | SSE |
| 127.5918 | 127.5918 | 185.5791 | HYBRID |
| 6.3796 | 6.3796 | 9.2789 | Chi square |
| 2.3751 | 2.3751 | 2.8360 | SNE |
| Freundlich isotherm |  |  |  |
| 64.4087 | 64.4080 | 67.5192 | KF |
| 0.9699 | 0.9699 | 1 | nF |
| 75.9017 | 75.9016 | 70.1730 | SSE |
| 127.6910 | 127.6910 | 140.4557 | HYBRID |
| 6.3845 | 6.3846 | 7.0228 | Chi square |
| 2.4141 | 2.4141 | 2.9245 | SNE |
| D-R isotherm |  |  |  |
| 25.8391 | 25.8391 | 23.8900 | qSD |
| 0.0382 | 0.0382 | 0.0317 | Kad |
| 63.3071 | 63.3071 | 56.9794 | SSE |
| 104.1891 | 104.1891 | 137.6983 | HYBRID |
| 5.2094 | 5.2094 | 6.8849 | Chi square |
| 2.5133 | 2.5133 | 2.9000 | SNE |
| R-P isotherm |  |  |  |
| 1679269 | 1465680 | 100.8481 | KR |
| 27824.32 | 24285.17 | 3.0590 | aR |
| 0 | 0 | 1 | g |
| 75.4271 | 75.4271 | 62.1031 | SSE |
| 128.0513 | 128.0513 | 185.5782 | HYBRID |
| 6.4026 | 6.4026 | 9.2789 | Chi square |
| 2.5560 | 2.5560 | 2.8233 | SNE |

Table 2

| Langmuir isotherm |  |  |  |
| --- | --- | --- | --- |
| Error function |  |  |  |
| Chi square | HYBRID | SSE |  |
| 144.1782 | 144.1782 | 46.1439 | qmL |
| 0.0016 | 0.0016 | 0.0064 | b |
| 5.5116 | 5.5116 | 4.7731 | SSE |
| 15.9550 | 15.9550 | 22.3910 | HYBRID |
| 0.7977 | 0.7977 | 1.1195 | Chi square |
| 2.4252 | 2.4252 | 2.8660 | SNE |
| Freundlich isotherm |  |  |  |
| 0.2179 | 0.2179 | 0.2181 | KF |
| 1 | 1 | 1 | nF |
| 6.0807 | 6.0807 | 6.0804 | SSE |
| 16.6676 | 16.6676 | 16.6682 | HYBRID |
| 0.8334 | 0.8334 | 0.8334 | Chi square |
| 2.9999 | 2.9999 | 2.9999 | SNE |
| D-R isotherm |  |  |  |
| 11.2121 | 11.2121 | 13.4360 | qSD |
| 17.8221 | 17.8221 | 50.2566 | Kad |
| 16.9670 | 16.9670 | 8.1904 | SSE |
| 47.6635 | 47.6635 | 75.6374 | HYBRID |
| 2.3832 | 2.3832 | 3.7819 | Chi square |
| 2.2603 | 2.2603 | 2.4827 | SNE |
| R-P isotherm |  |  |  |
| 21.5570 | 26.6966 | 0.3065 | KR |
| 91.4568 | 113.5035 | 0.0074 | aR |
| 0.0178 | 0.0178 | 1 | g |
| 7.4913 | 7.4914 | 6.2114 | SSE |
| 42.0166 | 42.0162 | 47.3484 | HYBRID |
| 2.1008 | 41.6836 | 6.6859 | Chi square |
| 1.9378 | 1.9043 | 1.9895 | SNE |

Table 3

| Langmuir isotherm |  |  |  |
| --- | --- | --- | --- |
| Error function |  |  |  |
| Chi square | HYBRID | SSE |  |
| 900 | 900 | 738.6743 | qmL |
| 0.0275 | 0.0275 | 0.0423 | b |
| 227.8484 | 227.8484 | 126.1830 | SSE |
| 496.6093 | 496.6093 | 601.6349 | HYBRID |
| 24.8305 | 24.8305 | 30.0817 | Chi square |
| 2.6509 | 2.6509 | 2.5538 | SNE |
| Freundlich isotherm |  |  |  |
| 28.1209 | 28.1209 | 29.9484 | KF |
| 0.7057 | 0.7057 | 1 | nF |
| 200.4758 | 200.4758 | 126.7146 | SSE |
| 403.5003 | 403.5003 | 574.8163 | HYBRID |
| 20.1750 | 20.1750 | 28.7308 | Chi square |
| 2.3318 | 2.3318 | 2.6321 | SNE |
| D-R isotherm |  |  |  |
| 173.7462 | 173.7462 | 13.4360 | qSD |
| 1.0253 | 1.0253 | 50.2566 | Kad |
| 182.0090 | 182.0090 | 2796.167 | SSE |
| 444.6280 | 444.6280 | 2666.644 | HYBRID |
| 17.7851 | 17.7851 | 106.6657 | Chi square |
| 0.3986 | 0.3986 | 3 | SNE |
| R-P isotherm |  |  |  |
| 937000.4 | 817818.7 | 202.0916 | KR |
| 38385.39 | 33502.84 | 5.7561 | aR |
| 0 | 0 | 0.0396 | g |
| 218.1445 | 218.1445 | 126.2006 | SSE |
| 1951.174 | 488.1460 | 605.5346 | HYBRID |
| 24.4073 | 97.5587 | 31.2714 | Chi square |
| 2.2502 | 1.0602 | 1.2094 | SNE |

Table 4

| Langmuir isotherm |  |  |  |
| --- | --- | --- | --- |
| Error function |  |  |  |
| Chi square | HYBRID | SSE |  |
| 16.6606 | 16.6606 | 15.4512 | qmL |
| 0.0292 | 0.0292 | 0.0385 | b |
| 9.9898 | 9.9898 | 8.7093 | SSE |
| 38.8881 | 38.8881 | 46.1521 | HYBRID |
| 1.9444 | 1.9444 | 2.3076 | Chi square |
| 2.6852 | 2.6852 | 2.8718 | SNE |
| Freundlich isotherm |  |  |  |
| 0.1544 | 0.1544 | 0.1410 | KF |
| 1 | 1 | 1 | nF |
| 63.8291 | 63.8291 | 60.6562 | SSE |
| 188.3103 | 188.3103 | 193.8583 | HYBRID |
| 9.4155 | 9.4155 | 9.6927 | Chi square |
| 2.9428 | 2.9428 | 2.9503 | SNE |
| D-R isotherm |  |  |  |
| 10.4108 | 10.4108 | 11.0042 | qSD |
| 13.2432 | 13.2432 | 15.1191 | Kad |
| 13.1342 | 13.1342 | 12.2304 | SSE |
| 32.4068 | 32.4068 | 35.2514 | HYBRID |
| 1.2963 | 1.2963 | 1.4100 | Chi square |
| 2.8386 | 2.8386 | 2.9312 | SNE |
| R-P isotherm |  |  |  |
| 62924.81 | 55005.74 | 1.1201 | KR |
| 40308.01 | 35235.2 | 0.2379 | aR |
| 0.5450 | 0.5450 | 0.7640 | g |
| 8.3535 | 8.3535 | 7.3263 | SSE |
| 17773811 | 46.1452 | 43.0236 | HYBRID |
| 2.3073 | 888690.5 | 989255.2 | Chi square |
| 2.0000 | 1.0500 | 1.8770 | SNE |

Table 5

| Initial Concentration (mgL) | 25 | 50 | 75 | 100 | 150 | 200 | 300 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorption capacity (mgg) | 1.2867 | 2.5672 | 3.9226 | 5.7742 | 8.8009 | 11.7562 | 16.2294 |

Table 6

| Initial Concentration (mgL) | 25 | 50 | 75 | 100 | 150 | 200 | 300 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| RL | 0.1366 | 0.0733 | 0.0494 | 0.0341 | 0.0226 | 0.017 | 0.0124 |