Supplemental information

Figure S1. The schematic illustration of the synthesis of the Na4FexP4O12+x (2≤x≤4) samples.

Figure S2. Rietveld refinement of the XRD pattern of the x = 2.70 sample.

Figure S3. Rietveld refinement of the XRD pattern of the x = 3.31 sample.

Figure S4. Enlarged XRD patterns from 6 to 35° of the x = 2.86, 2.91, and 3.00 samples.

Figure S5. Rietveld refinements of the XRD pattern of the x = 2.91 sample.

Figure S6. The IR spectra of a series of Na4FexP4O12+x samples (2≤x≤4).

Figure S7. The Raman spectrum of the NFPP (x = 2.91) sample.

Figure S8. The XPS spectrum of the NFPP (x = 2.91) sample.

Figure S9. Rietveld refinement of the XRD pattern of the x = 2.86 sample.

Figure S10. The CV curves of the NFPO (x = 2.00) electrode at a scan rate of 2 mV s-1.

Figure S11. The CV curves of the NFPP (x = 2.91) electrode at a scan rate of 2 mV s-1.

Figure S12. The rate performance of a series of Na4FexP4O12+x (2≤x≤4) electrodes.

Figure S13. The Na+ insertion/extraction kinetics of the NFPP (x = 2.91) electrode. (a) The CV curves of the NFPP electrode at different sweep rates. (b) The relationship between the peak current and the square root of the scan rates. (c) The logarithmic relationship between the peak current and scan rate. (d) The ratio of capacitive contribution at different sweep rates at 3.2 V.

The Na+ diffusion coefficient in the electrode can be calculated based on the following equation:

ip=2.69×105n3/2AD1/2C0v1/2

Where ip, n, A, D, C0 and v are the peak current (A), charge-transfer number (mol), interfacial contact area between electrolyte and electrode (cm2), Na+ diffusion coefficient (cm2 s-1), Na+ bulk concentration in electrode (mol L-1), and scan rate (mv s-1), respectively.1

The charge-storage mechanism is analyzed based on the following equations:

i=avb

logi=b×logv+loga

iV=k1v+k2v1/2

Where i, v, a, and b re peak current (A), scan rate (mv s-1), and adjustable parameters. When the b-value is 1 or around 0.5, it is indicative of a capacitive response or a diffusion limitation response, respectively (Angew. Chem. Int. Edit. 2021, 60, 21310).

Figure S14. The Na+ insertion/extraction kinetics of the NFPO (x = 2.00) electrode. (a) The CV curves of the NFPO electrode at different sweep rates. (b) The relationship between the peak current and the square root of the scan rates. (c) The logarithmic relationship between the peak current and scan rate. (d) The ratio of capacitive contribution at different sweep rates at 3.2 V.

Figure S15. The cycling stability of the HC//NFPP pouch cell from 0 to 3.6 V.

Table S1. The detailed raw material ratio of a series of Na4FexP4O12+x (2≤x≤4) samples and the ICP test results.

| Raw materials |  | Theoretical P/Fe ratio | Experimental P/Fe ratio (ICP) | Molecular formula (2≤x≤4) |
| --- | --- | --- | --- | --- |
| NaH2PO4·2H2O (mmol) | FeNO4·9H2O (mmol) |  |  |  |
| 4.00 | 2.00 | 2.00 | 1.99 | Na4Fe2.00P4Ox |
| 4.00 | 2.11 | 1.90 | 1.91 | Na4Fe2.11P4Ox |
| 4.00 | 2.25 | 1.78 | 1.78 | Na4Fe2.25P4Ox |
| 4.00 | 2.40 | 1.67 | 1.68 | Na4Fe2.40P4Ox |
| 4.00 | 2.55 | 1.57 | 1.57 | Na4Fe2.55P4Ox |
| 4.00 | 2.70 | 1.48 | 1.49 | Na4Fe2.70P4Ox |
| 4.00 | 2.86 | 1.40 | 1.40 | Na4Fe2.86P4Ox |
| 4.00 | 2.91 | 1.37 | 1.36 | Na4Fe2.92P4Ox |
| 4.00 | 3.00 | 1.33 | 1.33 | Na4Fe3.00P4Ox |
| 4.00 | 3.10 | 1.29 | 1.30 | Na4Fe3.10P4Ox |
| 4.00 | 3.15 | 1.27 | 1.27 | Na4Fe3.15P4Ox |
| 4.00 | 3.31 | 1.21 | 1.20 | Na4Fe3.31P4Ox |
| 4.00 | 3.45 | 1.16 | 1.16 | Na4Fe3.45P4Ox |
| 4.00 | 3.60 | 1.11 | 1.12 | Na4Fe3.60P4Ox |
| 4.00 | 3.74 | 1.07 | 1.06 | Na4Fe3.74P4Ox |
| 4.00 | 3.88 | 1.03 | 1.03 | Na4Fe3.88P4Ox |
| 4.00 | 4.00 | 1.00 | 1.00 | Na4Fe4.00P4Ox |

Table S2. Detailed structural information of the NFPO (x = 2.00) sample after the Rietveld refinement.

| Formula |  |  |  | Na2FeP2O7 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Crystal system |  |  |  | Triclinic |  |  |  |
| Space group |  |  |  | P-1 |  |  |  |
| a (Å) |  |  |  | 6.4279(19) |  |  |  |
| b (Å) |  |  |  | 9.4049(3) |  |  |  |
| c (Å) |  |  |  | 11.0126(4) |  |  |  |
| Unitcell volume (Å3 ) |  |  |  | 572.62(3) |  |  |  |
| Source |  |  |  | XRD |  |  |  |
| Wave length (Å) |  |  |  | 1.54056 |  |  |  |
| 2θ range |  |  |  | 5-55° |  |  |  |
| Rwp（%） |  |  |  | 6.9 |  |  |  |
| Atom | x | y | z |  | Uiso | Occ | Mult |
| Fe2 | 0.64908 | -0.01062 | 0.25993 |  | 0.02975 | 1 | 2 |
| P1 | 0.57578 | 0.22021 | 0.44864 |  | 0.01674 | 1 | 2 |
| P2 | 0.12592 | 0.03686 | 0.31841 |  | 0.00109 | 1 | 2 |
| P3 | 0.07126 | 0.33966 | 0.77756 |  | 0.01914 | 1 | 2 |
| P4 | 0.27453 | 0.68340 | 0.03326 |  | 0.00380 | 1 | 2 |
| Na1 | 0.02175 | 0.31944 | 0.47463 |  | 0.06315 | 1 | 2 |
| Na2 | 0.41068 | 0.64305 | 0.33782 |  | 0.03462 | 1 | 2 |
| Na3 | 0.24480 | 0.30516 | 0.13032 |  | 0.16943 | 1 | 2 |
| Na4 | 0.50000 | 0.00000 | 0.00000 |  | 0.16345 | 0.3333 | 2 |
| Na5 | 0.13762 | 0.02288 | 0.03395 |  | 0.10347 | 0.5 | 2 |
| Na6 | 0.42490 | 0.14878 | -0.23260 |  | -0.52560 | 0.3333 | 2 |
| O1 | -0.00560 | 0.24918 | 0.27920 |  | 0.02165 | 1 | 2 |
| O2 | 0.66740 | 0.35713 | 0.43779 |  | 0.02134 | 1 | 2 |
| O3 | 0.31937 | 0.01380 | 0.23054 |  | -0.02920 | 1 | 2 |
| O4 | 0.12597 | 0.41643 | 0.84358 |  | 0.01968 | 1 | 2 |
| O5 | 0.73853 | 0.06029 | 0.54414 |  | 0.01059 | 1 | 2 |
| O6 | 0.25194 | 0.19591 | 0.80644 |  | 0.01890 | 1 | 2 |
| O7 | 0.00505 | 0.07448 | 0.68769 |  | 0.00330 | 1 | 2 |
| O8 | 0.80237 | 0.43351 | 0.03145 |  | 0.06308 | 1 | 2 |
| O9 | 0.44359 | 0.57851 | 0.14665 |  | 0.02170 | 1 | 2 |
| O10 | 0.62022 | 0.21357 | 0.02719 |  | 0.05580 | 1 | 2 |
| O11 | 0.38971 | 0.20938 | 0.52142 |  | 0.07374 | 1 | 2 |
| O12 | 0.56572 | 0.16970 | 0.33602 |  | 0.01080 | 1 | 2 |
| O13 | 0.08360 | 0.77839 | 0.11142 |  | 0.01410 | 1 | 2 |
| O14 | 0.02461 | 0.60288 | 0.34131 |  | 0.00196 | 1 | 2 |

Table S3. Detailed structural information of the NFPP (x = 3.00) sample after the Rietveld refinement.

| Formula |  |  |  | Na4Fe3(PO4)2(P2O7) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Crystal system |  |  |  | Orthorhombic |  |  |  |
| Space group |  |  |  | Pn21a (No. 33) |  |  |  |
| a (Å) |  |  |  | 18.1020(11) |  |  |  |
| b (Å) |  |  |  | 6.5372(4) |  |  |  |
| c (Å) |  |  |  | 10.6496(7) |  |  |  |
| Unitcell volume (Å3 ) |  |  |  | 1260.13(14) |  |  |  |
| Source |  |  |  | XRD |  |  |  |
| Wave length (Å) |  |  |  | 1.54056 |  |  |  |
| 2θ range |  |  |  | 5-55° |  |  |  |
| Rwp（%） |  |  |  | 7.3 |  |  |  |
| Atom | x | y | z |  | Uiso | Occ | Mult |
| P1 | 0.29183 | 0.27922 | 0.48527 |  | -0.0023 | 1 | 4 |
| Fe3 | 0.23718 | 0.00838 | 0.74623 |  | 0.01910 | 1 | 4 |
| O13 | 0.44129 | -0.1917 | 0.84718 |  | 0.01645 | 1 | 4 |
| Fe1 | 0.33767 | -0.2276 | 0.50754 |  | 0.04205 | 1 | 4 |
| O14 | 0.39402 | -0.0942 | 0.69734 |  | 0.00661 | 1 | 4 |
| O4 | 0.24510 | 0.35900 | 0.38037 |  | 0.06830 | 1 | 4 |
| P4 | 0.45737 | -0.1801 | 0.74468 |  | 0.04274 | 1 | 4 |
| O9 | 0.50348 | -0.0427 | 0.65206 |  | 0.08807 | 1 | 4 |
| O5 | 0.24147 | -0.2337 | 0.63610 |  | -0.0412 | 1 | 4 |
| Fe2 | 0.13895 | 0.28857 | 0.50183 |  | -0.0029 | 0.95833 | 4 |
| O11 | 0.60675 | -0.0263 | 0.75554 |  | 0.04878 | 1 | 4 |
| P3 | 0.56248 | 0.16825 | 0.75472 |  | -0.0052 | 1 | 4 |
| Na1 | 0.50002 | 0.53847 | 0.99837 |  | 0.04121 | 1 | 4 |
| O6 | 0.11304 | -0.3910 | 0.51253 |  | -0.0427 | 1 | 4 |
| O12 | 0.58650 | 0.28264 | 0.62136 |  | 0.02083 | 1 | 4 |
| O2 | 0.34673 | 0.15692 | 0.48899 |  | 0.00600 | 1 | 4 |
| O3 | 0.35296 | 0.44641 | 0.57336 |  | -0.00012 | 1 | 4 |
| Na4 | 0.45821 | 0.41154 | 0.57825 |  | 0.02601 | 1 | 4 |
| O7 | 0.23622 | -0.2070 | 0.42788 |  | -0.02220 | 1 | 4 |
| P2 | 0.17656 | -0.2426 | 0.48321 |  | 0.02255 | 1 | 4 |
| O15 | 0.49789 | -0.3216 | 0.65409 |  | 0.02600 | 1 | 4 |
| Na2 | 0.30108 | 0.54048 | 0.75839 |  | 0.00481 | 1 | 4 |
| O1 | 0.23738 | 0.26564 | 0.62179 |  | 0.02422 | 1 | 4 |
| O8 | 0.14075 | -0.0620 | 0.49086 |  | 0.00420 | 1 | 4 |
| Na3 | 0.40666 | 0.08937 | 0.23531 |  | -0.0038 | 1 | 4 |
| O10 | 0.52587 | 0.28314 | 0.88827 |  | -0.0046 | 1 | 4 |

Table S4. Detailed structural information of the NFP (x = 4.00) sample after the Rietveld refinement.

| Formula |  |  |  | NaFePO4 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Crystal system |  |  |  | Orthorhombic |  |  |  |
| Space group |  |  |  | Pnma |  |  |  |
| a (Å) |  |  |  | 8.9821 |  |  |  |
| b (Å) |  |  |  | 6.8741 |  |  |  |
| c (Å) |  |  |  | 5.0482 |  |  |  |
| Unitcell volume (Å3 ) |  |  |  | 311.703 |  |  |  |
| Source |  |  |  | XRD |  |  |  |
| Wave length (Å) |  |  |  | 1.54056 |  |  |  |
| 2θ range |  |  |  | 5-55° |  |  |  |
| Rwp（%） |  |  |  | 6.4 |  |  |  |
| Atom | x | y | z |  | Uiso | Occ | Mult |
| Fe1 | 0.50000 | 0.50000 | 0.50000 |  | 0.02760 | 4 | 2 |
| P1 | 0.32147 | 0.25000 | 0.03194 |  | 0.02020 | 4 | 2 |
| Na1 | 0.64618 | 0.25000 | -0.03170 |  | 0.01947 | 4 | 2 |
| O1 | 0.37666 | 0.43155 | 0.17963 |  | 0.01788 | 4 | 2 |
| O2 | 0.37914 | 0.2500(0 | 0.75052 |  | 0.03315 | 4 | 2 |
| O3 | 0.15298 | 0.25000 | 0.04925 |  | 0.02276 | 8 | 2 |

Table S5. Detailed structural information on of the NFPP (x = 2.91) sample after the Rietveld refinement.

| Formula |  |  |  | Na4Fe2.91(PO4)2(P2O7) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Crystal system |  |  |  | Orthorhombic |  |  |  |
| Space group |  |  |  | Pn21a (No. 33) |  |  |  |
| a (Å) |  |  |  | 18.1193(9) |  |  |  |
| b (Å) |  |  |  | 6.5417(4) |  |  |  |
| c (Å) |  |  |  | 10.6564(6) |  |  |  |
| Unitcell volume (Å3 ) |  |  |  | 1263.11(12) |  |  |  |
| Source |  |  |  | XRD |  |  |  |
| Wave length (Å) |  |  |  | 1.54056 |  |  |  |
| 2θ range |  |  |  | 5-55° |  |  |  |
| Rwp（%） |  |  |  | 7.3 |  |  |  |
| Atom | x | y | z |  | Uiso | Occ | Mult |
| P1 | 0.28882 | 0.45497 | 0.51472 |  | -0.0075 | 1 | 4 |
| Fe3 | 0.24203 | 0.21116 | 0.75357 |  | 0.00862 | 1 | 4 |
| O13 | 0.46156 | -0.0240 | 0.86519 |  | 0.01503 | 1 | 4 |
| Fe1 | 0.33770 | -0.0412 | 0.49924 |  | 0.01947 | 1 | 4 |
| O14 | 0.39201 | 0.17627 | 0.71284 |  | 0.01707 | 1 | 4 |
| O4 | 0.25223 | 0.52925 | 0.37396 |  | 0.03193 | 1 | 4 |
| P4 | 0.45191 | 0.05878 | 0.72183 |  | 0.02511 | 1 | 4 |
| O9 | 0.49399 | 0.32360 | 0.68449 |  | 0.09138 | 1 | 4 |
| O5 | 0.25647 | -0.0250 | 0.58654 |  | -0.0079 | 1 | 4 |
| Fe2 | 0.14114 | 0.47118 | 0.49706 |  | -0.0068 | 0.97832 | 4 |
| O11 | 0.60606 | 0.17634 | 0.73731 |  | 0.02149 | 1 | 4 |
| P3 | 0.56166 | 0.39514 | 0.76465 |  | -0.0017 | 1 | 4 |
| Na1 | 0.51312 | 0.78014 | 0.96913 |  | 0.04282 | 1 | 4 |
| O6 | 0.12367 | -0.2272 | 0.47108 |  | -0.0385 | 1 | 4 |
| O12 | 0.58747 | 0.48753 | 0.63088 |  | 0.01050 | 1 | 4 |
| O2 | 0.36649 | 0.32972 | 0.47954 |  | 0.00156 | 1 | 4 |
| O3 | 0.35213 | 0.65830 | 0.58299 |  | 0.05201 | 1 | 4 |
| Na4 | 0.47044 | 0.57268 | 0.56756 |  | 0.08449 | 1 | 4 |
| O7 | 0.21221 | 0.02015 | 0.41356 |  | 0.03608 | 1 | 4 |
| P2 | 0.16915 | -0.0876 | 0.52006 |  | 0.01036 | 1 | 4 |
| O15 | 0.48845 | -0.1414 | 0.62681 |  | 0.02843 | 1 | 4 |
| Na2 | 0.29434 | 0.71280 | 0.75957 |  | 0.00158 | 1 | 4 |
| O1 | 0.21845 | 0.42415 | 0.61503 |  | -0.0285 | 1 | 4 |
| O8 | 0.14386 | 0.12010 | 0.49316 |  | -0.0059 | 1 | 4 |
| Na3 | 0.39627 | 0.33411 | 0.24769 |  | -0.0113 | 1 | 4 |
| O10 | 0.53275 | 0.44735 | 0.87982 |  | -0.0200 | 1 | 4 |

Table S6. Detailed structural information of the NFPP (x = 2.86) sample after the Rietveld refinement.

| Formula |  |  |  | Na4Fe2.86(PO4)2(P2O7) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Crystal system |  |  |  | Orthorhombic |  |  |  |
| Space group |  |  |  | Pn21a (No. 33) |  |  |  |
| a (Å) |  |  |  | 18.1188(10) |  |  |  |
| b (Å) |  |  |  | 6.5424(4) |  |  |  |
| c (Å) |  |  |  | 10.6532(6) |  |  |  |
| Unitcell volume (Å3 ) |  |  |  | 1262.99(12) |  |  |  |
| Source |  |  |  | XRD |  |  |  |
| Wave length (Å) |  |  |  | 1.54056 |  |  |  |
| 2θ range |  |  |  | 5-55° |  |  |  |
| Rwp（%） |  |  |  | 7.3 |  |  |  |
| Atom | x | y | z |  | Uiso | Occ | Mult |
| P1 | 0.29173 | 0.44322 | 0.49451 |  | 0.00220 | 1 | 4 |
| Fe3 | 0.24329 | 0.20903 | 0.75832 |  | 0.00470 | 1 | 4 |
| O13 | 0.46457 | -0.0760 | 0.85435 |  | 0.02082 | 1 | 4 |
| Fe1 | 0.34018 | -0.0563 | 0.48728 |  | 0.01128 | 1 | 4 |
| O14 | 0.39999 | 0.20107 | 0.77536 |  | 0.05639 | 1 | 4 |
| O4 | 0.24342 | 0.51953 | 0.37377 |  | 0.08408 | 1 | 4 |
| P4 | 0.44917 | 0.04712 | 0.70481 |  | 0.03106 | 1 | 4 |
| O9 | 0.49557 | 0.30536 | 0.68085 |  | 0.14291 | 1 | 4 |
| O5 | 0.25708 | -0.0219 | 0.58222 |  | -0.0114 | 1 | 4 |
| Fe2 | 0.14205 | 0.46326 | 0.50033 |  | -0.0149 | 0.97562 | 4 |
| O11 | 0.61248 | 0.11536 | 0.73578 |  | 0.01494 | 1 | 4 |
| P3 | 0.56309 | 0.38211 | 0.76804 |  | -0.0152 | 1 | 4 |
| Na1 | 0.50284 | 0.75264 | 0.98091 |  | 0.04973 | 1 | 4 |
| O6 | 0.13199 | -0.2411 | 0.45774 |  | -0.0438 | 1 | 4 |
| O12 | 0.57716 | 0.42783 | 0.63829 |  | 0.00979 | 1 | 4 |
| O2 | 0.36802 | 0.32207 | 0.47457 |  | -0.0047 | 1 | 4 |
| O3 | 0.35362 | 0.66347 | 0.57908 |  | 0.02399 | 1 | 4 |
| Na4 | 0.46848 | 0.54462 | 0.56969 |  | 0.03040 | 1 | 4 |
| O7 | 0.20970 | 0.05168 | 0.41695 |  | 0.00808 | 1 | 4 |
| P2 | 0.16959 | -0.0735 | 0.51703 |  | 0.02988 | 1 | 4 |
| O15 | 0.48605 | -0.1618 | 0.64431 |  | 0.06744 | 1 | 4 |
| Na2 | 0.29495 | 0.70750 | 0.76233 |  | 0.0053 | 1 | 4 |
| O1 | 0.23040 | 0.42342 | 0.61058 |  | 0.00541 | 1 | 4 |
| O8 | 0.12949 | 0.14405 | 0.46449 |  | -0.0318 | 1 | 4 |
| Na3 | 0.39555 | 0.31872 | 0.25335 |  | -0.0137 | 1 | 4 |
| O10 | 0.54072 | 0.42506 | 0.89563 |  | -0.0255 | 1 | 4 |