Supporting Material for

Enhanced Phase-Change Condensation Using Inverse Opals

Solomon Adera,1,2,5, * Nikolaj K. Mandsberg,4, Lauren Naworski,1 Anna V. Shneidman,1 Jack Alvarenga2, Joanna Aizenberg1,2,3, *

1John A. Paulson School of Engineering and Applied Sciences, Harvard University, Cambridge, Massachusetts 02138, USA.

2Wyss Institute for Biologically Inspired Engineering, Harvard University, Cambridge, Massachusetts 02138, USA.

3Department of Chemistry and Chemical Biology, Harvard University, Cambridge, Massachusetts 02138, USA.

4Department of Micro- and Nanotechnology, Technical University of Denmark, 2800 Kongens Lyngby, Denmark

5Department of Mechanical Engineering, University of Michigan, Ann Arbor, Michigan 48109, USA.

Address correspondence to sadera@umich.edu and jaiz@seas.harvard.edu

S1. Surface characterization

A copper plate was coated with silica inverse opals using the same colloidal co-assembly technique used for the copper tubes.1-3 The apparent contact angle of a millimeter-size water droplet was measured using a digital shape analyzer (DSA100, KRÜSS GmbH). Before silane treatment, water spreads instantaneously with vanishing (near zero) contact angle (Fig. S1a). When the inverse opal coated copper plate was silanized (hydrophobized via silane treatment), the water droplet remained contained with advancing/receding contact angle of 155°/142° (~13° contact angle hysteresis) (Fig. S1b). When the silanized porous inverse opals were impregnated with silicone oil (100 cSt at 25 °C), the droplet became hemispherical with ~90° apparent contact angle (Fig. S1c). The advancing/receding contact angle of a millimeter-size water droplet on the nanostructured lubricated surface was 95°/94° with ~1° contact angle hysteresis.

Figure S1. Contact angle. Apparent contact angle of a millimeter size water droplet on a copper plate coated with porous silica inverse opals (a) before silanization, (b) after silanization, and (c) after oil impregnation. Due to the inherent hydrophilicity of silica, water spreads instantaneously with near zero degree contact angle. When the surface was hydrophobized with silane, the advancing/receding contact angle became 155°/142°. When the hydrophobized silica nanopores were impregnated with a lubrication film, the advancing/receding contact angle became 95°/94° with ~1° contact angle hysteresis.

More than 15 condensation experiments, each lasting 3-4 hr, were conducted on the inverse opal coated copper tubes. No heat transfer performance degradation was observed in our experiments. Additionally, we used SEM to investigate the surface coating (topography) post condensation. As shown in Fig. S2, the inverse opal coating and surface morphology was nearly intact after repeated (>15) condensation experiments. Visually, we did not observe wear and tear on the silica inverse opal coating.

Figure S2. SEM at different magnifications. (a-c) Top-down SEM of the inverse opal coating post condensation shows no visible damage or surface degradation. The inverse opal coating remained on the outer surface of the copper tube after hours of repeated (>15) condensation experiments. In repeated experiments, the copper tubes maintained high phase-change heat transfer rates.

S2. Environmental chamber

A stainless steel cylindrical environmental chamber shown schematically in Fig. S3 was built to experimentally characterize the heat transfer performance of the copper tubes. The environmental chamber was designed to maintain saturated conditions (saturation temperature and pressure) by eliminating NCGs from the system. The nominal diameter and length of the chamber are 15 cm and 45 cm, respectively. The chamber has two flanges (QF100-BK, KJLC) and gasket center rings (QF100−SAVR) to cover the right and left ends of the cylinder using clamps (QF-SDC-AL1). A resistive heating cable with a controller (3641K22, McMaster-Carr) is wrapped around the chamber to heat the walls slightly above saturation temperature to prevent condensation on the internal walls. To reduce heat loss to ambient air, the chamber is insulated externally. Calibrated Type K thermocouples (KMQSS-062G-6, Omega Engineering) are fed into the chamber via a thermocouple feedthrough (TFT3KY00008A) to measure wet-bulb and dry-bulb temperatures. Additionally, the chamber pressure is measured using a calibrated pressure transducer (275 Mini-Convectron®, MKS instruments).

Hot steam is supplied to the environmental chamber from a custom-made stainless steel vapor generator. A rope heater with a controller is wrapped around the stainless steel vapor generator (diameter ≈ 10 cm, length ≈ 30 cm). The vapor generator along with the rope heater are insulated externally to minimize heat loss to the surrounding air. The vapor supply line is heated using a separate rope heater to prevent steam condensation inside the flexible tubing (321-4-×-24, Swagelok) before reaching the chamber. A stainless steel needle valve (SS-4BG, Swagelok) is used to control the amount of vapor (hot steam) entering the chamber through a flange (QF16X4SWG).

In preparation for the experiment, the vapor generator was filled with DIW. The water in the vapor generator was degassed via boiling. The valve connecting the vapor generator and chamber was closed and the rope heater was turned on to boil the water vigorously. After boiling the water for 1-2 min, the pressurized vapor was allowed to escape by opening the valve. Following the pressure release, the valve was closed and the water was boiled for an additional 1-2 min before letting the vapor out again by opening the valve. This procedure was repeated at least 4-5 times before closing the valve and allowing the vapor/liquid mixture inside the vapor generator to reach saturation condition (~85 °C and 59 kPa) by turning off the power supply to the rope heater. The vapor/liquid saturation temperature inside the vapor generator was measured by inserting a calibrated Type K thermocouple. During the experiment, the temperature of the water/vapor mixture was maintained nearly constant at ~85 °C by adjusting the power regulating knob on the rope heater.

Chilled water was fed into the environmental chamber through a liquid feedthrough (LFT8B22SWSW). After attaching the copper tube in the water circulation line using union tee fittings (SS-400-3, Swagelok), the entire system was evacuated using a roughing pump (Edwards RV8, Mass-Vac Inc.). A cold trap (TLR4XI100QF) filled with liquid nitrogen was used to capture water vapor that would otherwise contaminate the oil in the vacuum pump. Chamber pressure was below ambient (negative absolute pressure) with negligible leak rate (<3 Pa/h). A bellow valve (SA0100MVQF), which connects the environmental chamber with the vacuum pump, remained closed during experiment. A separate bellow valve was used to rush air in and bring the chamber to atmospheric pressure after each experimental run which lasted for 3-4 hr. During experiment, the condensate that accumulated at the bottom surface was drained through a drain valve that is located at the bottom of the chamber.  After each experimental run, the internal walls of the chamber were dried using Kimwipes (Kimberly-Clark Professional™ 34155, Thermo Fisher Scientific) in preparation for the next experiment.

The environmental chamber has a 4 cm diameter sapphire viewing port (QF40-150-VP). A fiber optic illuminator (SCHOTT-KL1500-LCD, Leica Inc.) is used as a cold light source and DSLR camera (EOS 60D, Canon Inc.) is used to capture images of droplet nucleation, growth, and departure. All tubings except the copper tube were insulated to avoid condensation. The copper tube was maintained below the saturation temperature by circulating chilled water from a water bath heat exchanger (Haskris R050 Recirculating Chiller, Haskris). The flow rate of the cooling water was measured using a factory-calibrated liquid flow meter (10 LPM MAX, Alicat Scientific). Additionally, the temperature of the incoming and outgoing cooling water was measured using calibrated Type J thermocouples (JMQSS-062G-6, Omega Engineering). The data from the thermocouples, pressure transducer and flow meter were recorded using a data acquisition system (cDAQ-9174, CompactDAQ, National Instruments) that was interfaced with LabVIEW (National Instruments). Steady-state condition was reached when the fluctuation in temperature (wet-bulb, dry-bulb, inlet, and outlet temperatures) and chamber pressure were ≤0.25 °C/min and ≤0.1 kPa/min, respectively. Steady-state data was collected for ~3-5 min and time averaged for this study.

Figure S3. Schematic experimental setup. After attaching the copper tube to a chilled water line, the entire system was evacuated using a roughing pump to remove NCGs. Hot steam was supplied to the chamber from a vapor generator which was degassed via boiling prior to experiment. All tubings except the copper tube were insulated and the chamber walls were slightly heated above the saturation temperature to avoid condensation anywhere but the copper tube. The environmental chamber was insulated to minimize heat loss to ambient air. Images of droplet nucleation, growth, and departure were captured through the viewing port using a DSLR camera.

Depending on the surface functionalization, we observed different modes of condensation (Fig. S4). When the smooth copper tube was plasma treated, steam condensed in filmwise mode (Fig. S4a). When the smooth copper tube was hydrophobized, vapor condensed in dropwise mode (Fig. S4b). When the copper tube was coated with silica inverse opals, the condensate seeped into the porous media. Unlike filmwise condensation, the condensate was transported preferentially in the axial direction towards the ends of the tube through the cracks which provide a less resistant flow path (Fig, S4c). Arrows in Fig. S4c indicate the preferential axial condensate transport direction. When the copper tube was impregnated with silicone oil, steam condensed by forming discrete water droplets that depart early at smaller radius and higher frequency (Fig. S4d).

Figure S4. Modes of condensation. Photographic images of (a) filmwise condensation (FWC) on smooth plasma treated (hydrophilic), (b) dropwise condensation (DWC) on smooth hydrophobized (silane treated), (c) inverse opal condensation (IOC) on silica inverse opal coated, and (d) SLIPS condensation on oil-impregnated copper tubes.

S3. Thermocouple calibration

All thermocouples were calibrated prior to experiment by inserting them in a constant temperature water bath and correlating the thermocouple reading with the actual temperature. The water bath was maintained at constant temperature by recirculating the working fluid (Lauda ECO RE 420 G, LAUDA-Brinkmann). The refrigerant cooled heat exchanger has a built-in temperature controller with <0.05 °C accuracy. After setting the temperature on the controller, the working fluid was recirculated by connecting the inlet to the outlet. The thermocouples in the water bath were allowed to reach steady-state (<0.1°C/min) before collecting calibration data using a data acquisition system. The reading from the thermocouple (y-axis,) and the actual/true water bath temperature (x-axis) correlate linearly with <1% root-mean-square error (RMSE) as shown in Fig, S5. Error bars (one standard deviation) are small and not visible in Fig, S5. During experiments, the slope (α) and y-intercept (β) of the calibration curve were used as correction factors to deduce the actual/true temperature (Tact) from the thermocouple reading (Trdg) by using the equation

|  | Tact=Trdg-βα. |  |
| --- | --- | --- |

Figure S5. Thermocouple calibration curve. Thermocouples were calibrated prior to experiment by immersing them in a constant temperature water bath. The temperature reading from the thermocouple (Trdg) and the actual/true temperature (Tact) correlate linearly with <1% root-mean-square error (RMSE).

S4. Heat transfer model

The wet-bulb temperature was measured by inserting a calibrated thermocouple into a wet cloth that was Kapton taped (7648A726, MaMaster-Carr) at the bottom of the cylindrical chamber while the dry-bulb temperature was measured by hanging a thermocouple probe inside the chamber near the condensing copper tube. The configuration of these two thermocouple probes (wet-bulb and dry-bulb) is shown schematically in Fig. S6. In our experiment, the wet-bulb and dry-bulb temperatures match within the measurement uncertainty (±0.2 °C), indicating saturated condition (absence of NCGs) inside the environmental chamber. The saturation temperature, which was used in subsequent calculations, was deduced by linearly averaging the wet-bulb and dry-bulb temperatures.

Figure S6. Wet-bulb and dry-bulb temperatures. The wet-bulb temperature was measured by imbedding a thermocouple probe inside a wet cloth while the dry-bulb temperatures was measured by hanging a thermocouple probe near the condensing copper tube inside the environmental chamber. The wet-bulb and dry-bulb temperatures match within ±0.2 °C, indicating saturated conditions inside the chamber.

The temperatures of the incoming (T1) and outgoing (T2) cooling water were measured using calibrated Type J thermocouples (JMQSS-062G-6, Omega Engineering). Additionally, the volumetric flow rate was measured using a liquid flow meter. The heat rejected by the vapor as it condenses on the copper tube was obtained from the sensible heat gained by the circulating chilled water. The heat released per unit area or condensation heat flux (q") is given by

|  | q"=ρwVcwT2-T1πdoL, |  |
| --- | --- | --- |

where ρw, V, and cw are density, volumetric flow rate and specific heat capacity of the cooling water, respectively, do is the outer diameter (6.35 mm) and L is the length of the copper tube (60 mm). Since the phase-change heat transfer in our experiments is neither isothermal nor isoflux, we used logarithmic mean temperature difference (ΔTLMTD) as the average subcooling as

|  | ΔTLMTD=T2-Tv-T1-TvlnT2-TvT1-Tv, |  |
| --- | --- | --- |

where Tv is the vapor temperature (average of wet-bulb and dry-bulb). Accounting for the forced convection internal flow, conduction through the wall, and phase-change condensation outside the tube, the overall heat transfer coefficient (Uo) is given by

|  | Uo=q"ΔTLMTD. |  |
| --- | --- | --- |

We estimate the heat transfer coefficient for internal flow by first calculating the diameter-based Reynolds number (ReD) from the mass flow rate as

|  | ReD=4mwπdiμw, |  |
| --- | --- | --- |

where di is the internal diameter (4.57 mm), μw is the viscosity of water, and mw is mass flow rate which can be obtained easily from the measured volume flow rate as

|  | mw=ρwV. |  |
| --- | --- | --- |

To minimize the internal flow (convection) resistance, we used large flow rates (≥5 LPM) which resulted in turbulent flow with ReD>10,000. The friction factor (f) was obtained from the Reynolds number using the Petukhov’s correlation for turbulent flow4 as

|  | f=0.790 lnReD-1.64-2. |  |
| --- | --- | --- |

The dimensionless diameter-based Nusselt number (NuD) was estimated from the friction factor (f) and Reynolds number (ReD) using the Gnielinski correlation for pipe flow4 as

|  | NuD=f8ReD-1000Pr1+12.7f81/2Pr2/3-1, |  |
| --- | --- | --- |

where Pr is the dimensionless Prandtl number (ratio of momentum to thermal diffusivity). The internal heat transfer coefficient (hi) was calculated from the Nusselt number as

|  | hi=NuDkwdi, |  |
| --- | --- | --- |

where kw is the thermal conductivity of water.

Knowing the convection and the conduction resistances, the steady-state phase-change condensation heat transfer coefficient on the vapor-side (hc) was calculated as

|  | hc=1Uo-AoAihi-Aolndo/di2πLkt-1, |  |
| --- | --- | --- |

where kt is the thermal conductivity of the tube, Ai and A0 are the inner (πdiL) and outer (πdoL) surface areas of the tube, respectively.

Rearranging Eq. (10) gives three thermal resistances in series as

|  | 1AoUo=1Aihi+lndo/di2πLkt+1Aohc, |  |
| --- | --- | --- |

where the left side of the equation represents the overall thermal resistance (1/AoUo). The first (1/Aihi) and last (1/Aohc) terms represent the thermal resistances associated with forced internal flow and phase-change condensation, respectively. The middle term (lndo/di/2πLkt) represents the conduction resistance through the walls of the tube in the radial direction. The internal wall temperature of the tube (Tw,i) can be computed as

|  | Tw,i=Tb+QAihi, |  |
| --- | --- | --- |

where Q is the total heat rejected by the vapor (mwcwT2-T1) and Tb is the bulk temperature of the chilled water which can be estimated by averaging the inlet and outlet water temperatures as 12T1+T2. Similarly, the outside wall temperature (Tw,o) can be estimated as

|  | Tw,o=Tw,i+Q lndo/di2πLkt. |  |
| --- | --- | --- |

The temperature difference between the condensing outer wall (Tw,o) and the saturated vapor inside the chamber (Tv) is the actual/true subcooling which is given by

|  | ΔT=Tv-Tw,o. |  |
| --- | --- | --- |

where ΔT is subcooling.

S5. Modeling Nusselt laminar film condensation

The phase-change heat transfer coefficient for laminar filmwise condensation (hc,FWC) is given by the classical Nusselt model4,5 as

|  | hc,fwc=0.728gρwρw-ρvkw3hfg'μwdoTv-Tw,o1/4, |  |
| --- | --- | --- |

where g is the acceleration due to gravity (9.81 m/s2) and hfg' is the modified latent heat of vaporization which can be estimated as

|  | hfg'=hfg+0.68cwTv-Tw,o. |  |
| --- | --- | --- |

In Eq. (16), hfg is the latent heat of vaporization evaluated at the wall temperature (Tw,o).

S6. Error propagation analysis

The measurement uncertainty on the overall heat transfer coefficient (Uo) is calculated by propagating the instrument uncertainty of each measured quantity. This is given by

|  | SUoUo=Smwmw2+ST2-T1T2-T12+-SAoAo2+-SΔTLMTDΔTLMTD2. |  |
| --- | --- | --- |

As the phase-change heat transfer coefficient (hc) is a product of powers, the measurement error is estimated by taking the first partial derivatives of hc with respect to the overall and internal heat transfer coefficients as

|  | Shchc=∂hc∂UoSUoUo2+∂hc∂hiShihi2. |  |
| --- | --- | --- |

The first partial derivatives of hc with respect to the overall heat transfer coefficient (Uo) and internal convection heat transfer coefficient (hi) are given by

|  | ∂hc∂Uo=hi2hi-Ao/AiUo-RtAoUohi2, |  |
| --- | --- | --- |

and

|  | ∂hc∂hi=-Ao/AiUo2hi-Ao/AiUo-RtAoUohi2, |  |
| --- | --- | --- |

where Rt is the conduction resistance of the tube in the radial direction. The radial conduction resistance for the cylindrical tube is given by

|  | Rt=lndo/di2πkt. |  |
| --- | --- | --- |

The error bars reported in this study are obtained by combining system and random errors for one standard deviation. Table S1 summarizes the uncertainty associated with each measured quantity.

Table S1. Uncertainties corresponding to experimental measurement.

| Experimental measurement | Uncertainty (±) |
| --- | --- |
| Calibrated thermocouples (T1, T2, Tv) | <0.2 K |
| Saturated vapor pressure (Pv) | <2% |
| Chilled water mass flow rate (mw) | <4% |
| Copper tube surface area (Ao, Ai) | <2% |
| Gnielinski correlation heat transfer coefficient (hi) | <10% |

References

1	Hatton, B., Mishchenko, L., Davis, S., Sandhage, K. H. & Aizenberg, J. Assembly of large-area, highly ordered, crack-free inverse opal films. Proc. Natl. Acad. Sci. U. S. A. 107, 10354-10359 (2010).

2	Mishchenko, L., Hatton, B., Kolle, M. & Aizenberg, J. Patterning hierarchy in direct and inverse opal crystals. Small 8, 1904-1911 (2012).

3	Phillips, K. R. et al. Fabrication of photonic microbricks via crack engineering of colloidal crystals. Adv. Funct. Mater. 30, 1908242-1908211 (2020).

4	Mills, A. F. Basic Heat and Mass Transfer. 2nd edn,  (Prentice-Hall, 1999).

5	Nusselt, W. Die Oberflachenkondensation des Wasserdamphes. Zeitschrift Des Vereines Deutscher Ingenieure 60, 541-546 (1916).