Supporting Information

Superatomic Icosahedral-CnB12-n (n = 0, 1, 2) Stuffed Mononuclear and Binuclear Borafullerene and Borospherene Nanoclusters with Spherical Aromaticity

Min Zhang, Wei-Ping Jia, Ting Zhang, Bin-Bin Pei, Jia Xu, Xinxin Tian, Hai-Gang Lu*, and Si-Dian Li*

Institute of Molecular Science, Shanxi University, Taiyuan 030006, China

Contents

Figure S1 Structural constructions of mononuclear Ih B104, Ci C50B54 (1)，C1 C50B54

(2), and S10 C50B54 (3) based on the structural motif of Ih C80.

Figure S2 Structural constructions of binuclear Cs C88B78 (4), Cs C88B78 (5), and Cs

C88B78 (6) based on the structural motifs of Ih C80 and D5d C120.

Figure S3 Structural constructions of binuclear Cs B180 (7)，Cs B182 (8)，and Cs B184 (9) based on the structural motifs of Ih C70 and C2v C110.

Figure S4 Relative energies of low-lying isomers of C50B54.

Figure S5 Relative energies of low-lying isomers of C88B78.

Figure S6 Relative energies of low-lying isomers of B184.

Figure S7 Optimized structures of C1 C50B34 and C2h C50B34 based on the structural motif of Ih C60 and optimized structure of C5 C50B44 based on the structural motif of D5h C70 .

Figure S8 Calculated cohesive energy per atom (Ec, eV/atom) of the optimized core-shell boron clusters Bn (n = 110-192) as a function of the cluster size (n) at TPSSh/6-311G(d) level.

Figure S9 BOMD simulations of (a) Ci C50B54 (1) at 1500K, (b) S10 C50B54 (3) at 1500K, and (c) Cs B184 (9) at 500K.

Figure S10 The superatomic electronic configuration 1S21P61D101F8 of carborane D5d C2B10H12.

Figure S11 AdNDP bonding analysis of S10 C50B54 (3).

Figure S12 Superatomic bonding orbitals of the two icosahedral B12 cores in Cs B182

(8) and Cs B184 (9).

Table S1 Calculated formation energies per atom and HOMO-LUMO gaps of the optimized borafullerenes C50B54 (1, 2, 3) and C88B78 (4, 5, 6) and the calculated NICS values (in ppm) at the geometric centers of the icosahedral-CnB12-n cores in them.

Table S2 Calculated cohesive energies per atom and HOMO-LUMO gaps of the optimized core-shell borospherenes Bn (n = 176-188) and the calculated NICS values (in ppm) at the geometric centers of icosahedral-B12 cores in them.

- Table S3 Optimized coordinates (x, y, z) of Ci C50B54 (1), C1 C50B54 (2), S10 C50B54 (3), Cs C88B78 (4), Cs C88B78 (5), Cs C88B78 (6), Cs B180 (7), Cs B182 (8) and Cs B184 (9) at PBE0/6-311G(d) level.

Fig. S1 Structural constructions of mononuclear Ih B104, Ci C50B54 (1)，C1 C50B54 (2)，and S10 C50B54 (3) based on the structural motif of Ih C80, with the icosahedral-CnB12-n (n = 0, 1, 2) cores at the center highlighted in pink.

Fig. S2 Structural constructions of binuclear Cs C88B78 (4)，Cs C88B78 (5)，and Cs C88B78 (6) based on the structural motifs of Ih C80 and D5d C120, with the interconnected icosahedral-CnB12-n (n = 0, 1, 2) cores at the center highlighted in pink.

Fig. S3 Structural constructions of binuclear Cs B180 (7), Cs B182 (8), and Cs B184 (9) based on the structural motifs of Ih C70 and C2v C110, with the interconnected icosahedral-B12 (n = 0, 1, 2) cores at the center highlighted in pink.

Fig. S4 Relative energies of the low-lying isomers of C50B54 at PBE0/6-31G(d) and PBE0/6-311G(d) (in parentheses) levels in eV.

Fig. S5 Relative energies of the low-lying isomers of C88B78 at PBE0/6-31G(d) and PBE0/6-311G(d) (in parentheses) levels in eV.

Fig. S6 Relative energies of the low-lying isomers of B184 at PBE0/6-31G(d) and PBE0/6-311G(d) (in parentheses) levels in eV.

Fig. S7 (a) Optimized structures of C1 C50B34 obtained in this work and C2h C50B34 from Ref. 41 based on the structural motif of Ih C60, with relative energies indicated in eV. (b) Optimized structure of C5 C50B44 constructed in the work based on the structural motif of D5h C70 at PBE0/6-311G(d) level.

Fig. S8 Calculated cohesive energy per atom (Ec, eV/atom) of the optimized core-shell boron clusters Bn (n = 110-192) as a function of the cluster size (n) at TPSSh/6-311G(d) level.

Fig. S9 BOMD simulations of (a) Ci C50B54 (1) at 1500K, (b) S10 C50B54 (3) at 1500K, and (c) Cs B184 (9) at 500 K, with the calculated average root−mean−square−deviations (RMSD) and maximum bond length deviations (MAXD) indicated.

Fig. S10 The superatomic electronic configuration 1S21P61D101F8 of carborane D5d C2B10H12 in canonical molecular orbitals.

Fig. S11 AdNDP bonding pattern of S10 C50B54(3) with the occuoation numbers indicated.

Fig. S12 The superatomic bonding orbitals of the two icosahedral B12 cores in Cs B182 (8) and Cs B184 (9) revealed by AdNDP analyses.

Table S1 Calculated formation energies (Ef) (in eV/atom) and HOMO-LUMO gaps (△Egap) (in eV) of the optimized borafullerenes C50B54 (1, 2, 3) and C88B78 (4, 5, 6) and the calculated NICS values (in ppm) at the geometric centers of the icosahedral-CnB12-n cores in them at PBE0/6-311G(d).

| Cluster(Symmetry) | PBE0 |  |  |
| --- | --- | --- | --- |
|  | Ef | NICS | △Egap |
| C50B54(Ci) (1) | -0.213 | -23.23 | 2.28 |
| C50B54(C1) (2) | -0.211 | -20.54 | 2.24 |
| C50B54(S10) (3) | -0.207 | -17.70 | 2.75 |
| C88B78(Cs) (4) | -0.209 | -32.47/-28.04 | 0.83 |
| C88B78(Cs) (5) | -0.204 | -29.06/-28.25 | 1.75 |
| C88B78(Cs) (6) | -0.189 | -28.39/-28.66 | 1.61 |

Table S2 Calculated cohesive energies per atom (Ec) (in eV/atom) and HOMO-LUMO gaps (△Egap) (in eV) of the optimized core-shell borospherenes Bn (n = 176-188) and the calculated NICS values (in ppm) at the geometric centers of icosahedral-B12 cores in them at PBE0/6-311G(d) level.

| Cluster(Symmetry) | PBE0 |  |  |
| --- | --- | --- | --- |
|  | -Ec | NICS | △Egap |
| B176(C1) | 5.668 | -29.52/-29.52 | 1.51 |
| B178(C1) | 5.678 | -27.80/-27.80 | 1.35 |
| B180(Cs) (7) | 5.681 | -30.95/-30.95 | 1.46 |
| B182(Cs) (8) | 5.679 | -28.32/-28.32 | 1.32 |
| B184(Cs) (9) | 5.691 | -32.68/-32.65 | 0.87 |
| B186(C5v) | 5.670 | -20.63/-20.63 | 1.21 |
| B188(Cs) | 5.673 | -25.27/-25.27 | 1.02 |

Table S3 Optimized coordinates (x, y, z) of Ci C50B54 (1), C1 C50B54 (2), S10 C50B54 (3), Cs C88B78 (4), Cs C88B78 (5), Cs C88B78 (6), Cs B180 (7), Cs B182 (8) and Cs B184 (9) at PBE0/6-311G(d) level.

Ci C50B54 (1)

B                 -0.04757300    2.86537500   -1.50473900

B                  0.04757300   -2.86537500    1.50473900

B                  1.70314700   -2.30417700   -1.50872400

B                  0.00741500   -0.04178400   -3.10049800

B                 -2.73228100    0.83475500   -1.50881300

B                 -1.70314700    2.30417700    1.50872400

B                  1.62589300    2.35749700    1.50822200

B                  2.70281200    0.92886000   -1.50668200

B                  2.73228100   -0.83475500    1.50881300

B                 -0.00741500    0.04178400    3.10049800

B                 -2.70281200   -0.92886000    1.50668200

B                 -1.62589300   -2.35749700   -1.50822200

B                  1.37316300    0.47381000   -0.73625500

B                  0.82905000    1.19949500    0.73446400

B                 -1.38979600    0.41840700   -0.73908100

B                 -0.87746700    1.16594200    0.73361600

B                  0.87746700   -1.16594200   -0.73361600

B                  1.38979600   -0.41840700    0.73908100

B                 -0.82905000   -1.19949500   -0.73446400

B                 -1.37316300   -0.47381000    0.73625500

B                 -0.02855300    1.45361700   -0.74123500

B                  0.02855300   -1.45361700    0.74123500

B                  1.64979800   -2.19260100    3.53030700

B                  2.58364300    0.88590900    3.55307300

B                 -0.06259700    2.87195700    3.61467800

B                 -1.55676000   -2.26107500    3.53182200

B                 -2.61505900    0.77509100    3.55800800

C                  0.02360800    4.37113600   -0.77048100

B                  2.54513900    3.42856400   -0.80818200

B                 -2.47227800    3.48189600   -0.80855500

C                  4.15261300    1.32772800   -0.76970800

B                  4.03602800   -1.36077000   -0.81508100

C                  2.54602700   -3.54722200   -0.76836200

B                 -0.04576100   -4.28932300   -0.81206800

C                 -2.58262200   -3.51601300   -0.76924800

B                 -4.06428200   -1.27487500   -0.81468900

C                 -4.13727500    1.37197500   -0.76951600

B                 -4.03602800    1.36077000    0.81508100

C                 -2.54602700    3.54722200    0.76836200

B                  0.04576100    4.28932300    0.81206800

C                  2.58262200    3.51601300    0.76924800

B                  4.06428200    1.27487500    0.81468900

C                  4.13727500   -1.37197500    0.76951600

B                  2.47227800   -3.48189600    0.80855500

C                 -0.02360800   -4.37113600    0.77048100

B                 -2.54513900   -3.42856400    0.80818200

C                 -4.15261300   -1.32772800    0.76970800

B                  0.06259700   -2.87195700   -3.61467800

B                  2.61505900   -0.77509100   -3.55800800

B                 -2.58364300   -0.88590900   -3.55307300

B                  1.55676000    2.26107500   -3.53182200

B                 -1.64979800    2.19260100   -3.53030700

C                  1.23704900   -0.31060800   -4.21874400

C                 -1.20392000   -0.42042400   -4.19539900

C                  0.69171600    1.06696100   -4.16815600

C                 -0.78197300    1.00081500   -4.16135700

C                  1.40075300   -3.26885700   -2.85595200

B                  2.70160800   -2.39088200   -2.96579200

B                 -1.43194600   -3.37053800   -2.96201100

C                 -2.61085000   -2.32567900   -2.85960400

C                  3.49869600    0.33979300   -2.85576100

C                  1.36198600   -3.95539100   -1.55037300

C                 -1.41800500   -4.01445800   -1.54547100

C                  3.35020600   -2.57304300   -1.55640500

C                 -3.30478400   -2.49796200   -1.56173200

C                  4.15540600    0.07687800   -1.55670700

B                  3.10986900    1.85152100   -2.95855300

B                 -3.61250700    0.33644800   -2.96309700

C                 -3.01964600    1.78483200   -2.85252100

C                  0.76056400    3.44260300   -2.85138700

B                 -0.79596900    3.54745800   -2.95754000

C                  3.48845600    2.40368000   -1.55135400

C                 -4.23592500    0.11116200   -1.55215200

C                 -3.40213000    2.38366500   -1.55352900

C                 -1.20613600    4.07022300   -1.54988300

C                  1.21413500    3.98507500   -1.55284800

C                 -1.21413500   -3.98507500    1.55284800

C                 -0.76056400   -3.44260300    2.85138700

C                 -3.48845600   -2.40368000    1.55135400

B                 -3.10986900   -1.85152100    2.95855300

C                  1.20613600   -4.07022300    1.54988300

B                  0.79596900   -3.54745800    2.95754000

C                  3.40213000   -2.38366500    1.55352900

C                  3.01964600   -1.78483200    2.85252100

C                  4.23592500   -0.11116200    1.55215200

B                  3.61250700   -0.33644800    2.96309700

C                 -4.15540600   -0.07687800    1.55670700

C                 -3.49869600   -0.33979300    2.85576100

C                  2.61085000    2.32567900    2.85960400

C                  3.30478400    2.49796200    1.56173200

C                 -3.35020600    2.57304300    1.55640500

B                 -2.70160800    2.39088200    2.96579200

C                 -1.36198600    3.95539100    1.55037300

C                 -1.40075300    3.26885700    2.85595200

B                  1.43194600    3.37053800    2.96201100

C                  1.41800500    4.01445800    1.54547100

C                 -1.23704900    0.31060800    4.21874400

C                  1.20392000    0.42042400    4.19539900

C                  0.78197300   -1.00081500    4.16135700

C                 -0.69171600   -1.06696100    4.16815600

C                 -0.00285900    0.00662900    1.55030000

C                  0.00285900   -0.00662900   -1.55030000

B                 -0.06195200    1.32720300    4.34461400

B                  0.06195200   -1.32720300   -4.34461400

C1 C50B54 (2)

B                 -0.84588100    2.82247900   -1.27265700

B                  0.84483900   -2.83127300    1.32939700

B                  2.33700000   -1.55950000   -1.54872500

B                  0.06878900    0.24936900   -3.13193600

B                 -2.82038300    0.12534400   -1.53359100

B                 -2.35810100    1.54599500    1.61022500

B                  0.85197300    2.58195400    1.76058600

B                  2.33938200    1.78167900   -1.28187800

B                  2.82744400   -0.13114400    1.58100600

B                 -0.10961400   -0.25360300    3.10881900

B                 -2.36780500   -1.76967800    1.34731400

B                 -0.85114200   -2.58508400   -1.70081700

B                  0.03285600    0.12393800   -1.56035800

B                  1.18498100    0.91081200   -0.59598000

B                  0.42039800    1.31737500    0.88794400

B                 -1.44167400    0.05083100   -0.72774800

B                 -1.20576200    0.78770300    0.80618400

B                  1.19316800   -0.79422500   -0.73199800

B                  1.43464400   -0.05877200    0.80000300

B                 -0.43117300   -1.32550900   -0.81082600

B                 -1.20035800   -0.91379200    0.67182000

B                 -0.44402700    1.43250400   -0.59234200

B                  0.43114000   -1.43923000    0.66811500

B                  2.15646400   -1.88123300    3.45210900

B                  2.15085000    1.31739600    3.70464200

B                 -0.91415600    2.31389300    3.74119000

B                 -0.90492100   -2.87682600    3.33290200

B                 -2.95730400   -0.28978400    3.54795400

C                 -1.22833300    4.24420700   -0.47076300

B                  1.45837500    4.05778600   -0.45408200

B                 -3.34839400    2.67102200   -0.67054700

C                  3.62303000    2.53078300   -0.50704900

B                  4.27720800   -0.07258400   -0.72771800

C                  3.49271200   -2.59666600   -0.91816000

B                  1.20970900   -4.01483700   -1.10148900

C                 -1.43973700   -4.04831100   -1.13567900

B                 -3.50371700   -2.32005900   -1.07333400

C                 -4.36061800    0.18146900   -0.87158300

B                 -4.30525700    0.07415500    0.72082300

C                 -3.47281700    2.58477000    0.90272500

B                 -1.21108000    4.01631700    1.11205100

C                  1.43594800    4.02756400    1.13039400

B                  3.51514900    2.32633000    1.07104400

C                  4.34195200   -0.17771200    0.85083500

B                  3.36283000   -2.67528100    0.66971000

C                  1.22679700   -4.22354400    0.46897100

B                 -1.45839500   -4.06137600    0.46276200

C                 -3.60582100   -2.51753400    0.49160300

B                  0.92432500   -2.29770200   -3.73155000

B                  2.79709200    0.28522800   -3.48615400

B                 -2.12052900   -1.31590900   -3.72062300

B                  0.91054400    2.86501200   -3.32092500

B                 -2.12930000    1.87704500   -3.46707800

C                  0.51489100   -0.83676500   -4.34383800

C                  1.34396200    0.37473000   -4.22966200

C                 -0.89779000   -0.42256800   -4.34146800

C                  0.44348400    1.53749800   -4.15617600

C                 -0.94194500    1.04474200   -4.22575800

C                  2.31475600   -2.42117100   -3.00033900

B                  3.33677500   -1.25018600   -2.99244100

B                 -0.33456700   -3.32797900   -3.23539400

C                 -1.76266600   -2.72659000   -3.11370000

C                  3.27817500    1.54082300   -2.66481100

C                  2.46459500   -3.23013800   -1.76622600

C                 -0.15747800   -4.09552900   -1.88916600

C                  3.99965000   -1.36860000   -1.58710900

C                 -2.40990700   -3.21294900   -1.87054400

C                  3.98029000    1.38654600   -1.36772800

B                  2.48624300    2.87806300   -2.68112300

B                 -3.45707000   -0.48043400   -3.08180100

C                 -3.31999800    1.05157500   -2.85043900

C                 -0.20169600    3.68739200   -2.56817600

B                 -1.71155900    3.35574800   -2.73486800

C                  2.67718500    3.42012800   -1.23234100

C                 -4.05081000   -0.99037700   -1.73367100

C                 -3.90731200    1.41772700   -1.53736800

C                 -2.29657800    3.65524500   -1.32137900

C                  0.04373400    4.25713200   -1.21931000

C                 -0.03837500   -4.26665700    1.22777100

C                  0.21084200   -3.73009200    2.58620300

C                 -2.67098700   -3.40782400    1.23325700

B                 -2.51507400   -2.88392500    2.70144700

C                  2.30267500   -3.64900300    1.31925600

B                  1.73033600   -3.38015400    2.74880000

C                  3.92385800   -1.41770500    1.53069800

C                  3.37237200   -1.05937500    2.85783300

C                  4.05805600    0.99307600    1.72163800

B                  3.50589800    0.48338100    3.08980700

C                 -4.01413600   -1.39490600    1.35695900

C                 -3.36803200   -1.55776900    2.67781200

C                  1.78689200    2.74874300    3.13097700

C                  2.41714500    3.21387300    1.87088700

C                 -4.01856300    1.37573400    1.57227800

B                 -3.41481000    1.26755800    3.00750200

C                 -2.46412000    3.22308800    1.77302100

C                 -2.34195500    2.43048300    3.02357900

B                  0.34554400    3.36333500    3.26026400

C                  0.16131800    4.09591300    1.89270200

C                 -0.48832800    0.87673300    4.28455300

C                  0.92705000    0.42777500    4.24624000

C                  0.96413800   -1.04493600    4.13622700

C                 -0.42700100   -1.56423500    4.11429500

C                 -0.04317000   -0.12748200    1.57467400

B                 -1.42470300   -0.37934700    4.31002900

S10 C50B54 (3)

B                 -0.05475100    2.84779700   -1.49818200

B                  0.05475100   -2.84779700    1.49818200

B                  1.71862100   -2.27274500   -1.49580200

B                  0.00044200   -0.00123200   -3.16113300

B                 -2.72565800    0.82773800   -1.49771100

B                 -1.71862100    2.27274500    1.49580200

B                  1.62963700    2.33703200    1.49643200

B                  2.69192100    0.93143700   -1.49740300

B                  2.72565800   -0.82773800    1.49771100

B                 -0.00044200    0.00123200    3.16113300

B                 -2.69192100   -0.93143700    1.49740300

B                 -1.62963700   -2.33703200   -1.49643200

B                  0.00025900   -0.00089300   -1.59316000

B                  1.37228500    0.48637400   -0.72679500

B                  0.82416000    1.20087600    0.72664900

B                 -1.39623500    0.41261600   -0.72739800

B                 -0.88725600    1.15519000    0.72627000

B                  0.88725600   -1.15519000   -0.72627000

B                  1.39623500   -0.41261600    0.72739800

B                 -0.00025900    0.00089300    1.59316000

B                 -0.82416000   -1.20087600   -0.72664900

B                 -1.37228500   -0.48637400    0.72679500

B                 -0.03871100    1.45540000   -0.72754200

B                  0.03871100   -1.45540000    0.72754200

B                  1.65180300   -2.16964300    3.56776200

B                  2.57370400    0.89992900    3.56805300

B                 -0.06073900    2.72548300    3.56818300

B                 -1.55323100   -2.24111500    3.56776500

B                 -2.61109900    0.78422500    3.56795800

C                  0.02702500    4.36970000   -0.78530700

B                  2.54548600    3.42061000   -0.80673900

B                 -2.46643700    3.47799700   -0.80652600

C                  4.16447900    1.32457600   -0.78536300

B                  4.03971700   -1.36408900   -0.80687400

C                  2.54712500   -3.55207700   -0.78567900

B                 -0.04912900   -4.26352700   -0.80703100

C                 -2.59078100   -3.52003000   -0.78561100

B                 -4.06993100   -1.27087000   -0.80697500

C                 -4.14777600    1.37602400   -0.78537900

B                 -4.03971700    1.36408900    0.80687400

C                 -2.54712500    3.55207700    0.78567900

B                  0.04912900    4.26352700    0.80703100

C                  2.59078100    3.52003000    0.78561100

B                  4.06993100    1.27087000    0.80697500

C                  4.14777600   -1.37602400    0.78537900

B                  2.46643700   -3.47799700    0.80652600

C                 -0.02702500   -4.36970000    0.78530700

B                 -2.54548600   -3.42061000    0.80673900

C                 -4.16447900   -1.32457600    0.78536300

B                  0.06073900   -2.72548300   -3.56818300

B                  2.61109900   -0.78422500   -3.56795800

B                 -2.57370400   -0.89992900   -3.56805300

B                  1.55323100    2.24111500   -3.56776500

B                 -1.65180300    2.16964300   -3.56776200

C                  0.06190100   -1.25241200   -4.28956400

C                  1.21040900   -0.32794000   -4.28925600

C                 -1.17216600   -0.44575400   -4.28885300

C                  0.68608200    1.04993900   -4.28847400

C                 -0.78629500    0.97713800   -4.28836400

C                  1.39012000   -3.20082100   -2.86060100

B                  2.70796400   -2.37753300   -2.96546400

B                 -1.42458000   -3.31037700   -2.96577900

C                 -2.61477500   -2.31131800   -2.86056700

C                  3.47438200    0.33319800   -2.86091700

C                  1.34854600   -3.92214300   -1.56083500

C                 -1.41369900   -3.99518800   -1.56045500

C                  3.36268500   -2.57909900   -1.56022800

C                 -3.31315600   -2.49456600   -1.56060300

C                  4.14698100    0.07058700   -1.56078800

B                  3.09863000    1.84102900   -2.96548300

B                 -3.58923600    0.33197900   -2.96596700

C                 -3.00690500    1.77267300   -2.86069700

C                  0.75678900    3.40751900   -2.86106000

B                 -0.79358900    3.51606900   -2.96585200

C                  3.49154100    2.40083800   -1.55983800

C                 -4.23626500    0.10981100   -1.56031300

C                 -3.39631000    2.38005300   -1.56033200

C                 -1.20459900    4.06248300   -1.55993200

C                  1.21410100    3.96554400   -1.56067200

C                 -1.21410100   -3.96554400    1.56067200

C                 -0.75678900   -3.40751900    2.86106000

C                 -3.49154100   -2.40083800    1.55983800

B                 -3.09863000   -1.84102900    2.96548300

C                  1.20459900   -4.06248300    1.55993200

B                  0.79358900   -3.51606900    2.96585200

C                  3.39631000   -2.38005300    1.56033200

C                  3.00690500   -1.77267300    2.86069700

C                  4.23626500   -0.10981100    1.56031300

B                  3.58923600   -0.33197900    2.96596700

C                 -4.14698100   -0.07058700    1.56078800

C                 -3.47438200   -0.33319800    2.86091700

C                  2.61477500    2.31131800    2.86056700

C                  3.31315600    2.49456600    1.56060300

C                 -3.36268500    2.57909900    1.56022800

B                 -2.70796400    2.37753300    2.96546400

C                 -1.34854600    3.92214300    1.56083500

C                 -1.39012000    3.20082100    2.86060100

B                  1.42458000    3.31037700    2.96577900

C                  1.41369900    3.99518800    1.56045500

C                 -1.21040900    0.32794000    4.28925600

C                 -0.06190100    1.25241200    4.28956400

C                  1.17216600    0.44575400    4.28885300

C                  0.78629500   -0.97713800    4.28836400

C                 -0.68608200   -1.04993900    4.28847400

Cs C88B78 (4)

B                  2.37681800   -0.69364500    1.63956300

B                 -2.25899600   -3.70315500   -1.59616400

B                 -0.90205100   -0.71698000   -2.84336400

B                 -0.90205100   -0.71698000    2.84336400

B                  0.86666900   -3.72741000    2.71229500

B                  2.92498600   -3.66312400    0.00000000

B                  2.37681800   -0.69364500   -1.63956300

B                  0.86666900   -3.72741000   -2.71229500

B                 -0.00599500   -5.27294100    0.00000000

B                 -2.25899600   -3.70315500    1.59616400

B                 -2.82674900   -0.66302100    0.00000000

B                  1.22462000   -1.50564400   -0.86156000

B                  1.49195700   -2.95717900    0.00000000

B                 -0.42271600   -1.44682000    1.42104000

B                  0.47965500   -2.94113000    1.38983100

B                 -0.42271600   -1.44682000   -1.42104000

B                  0.47965500   -2.94113000   -1.38983100

B                 -1.43491400   -1.48245500    0.00000000

B                 -1.12827600   -2.91594600    0.84818300

B                  1.22462000   -1.50564400    0.86156000

B                 -1.12827600   -2.91594600   -0.84818300

B                  1.75769100    0.91282900   -2.55307800

B                 -0.87679400    3.68744100    2.64668200

B                  1.75769100    0.91282900    2.55307800

B                 -2.64111600    0.77906500   -1.17105100

B                 -0.87679400    3.68744100   -2.64668200

B                  2.21750500    3.77748600   -1.63617400

B                  2.92169000    0.59713400    0.00000000

B                  2.21750500    3.77748600    1.63617400

B                 -0.02609300    5.25765600    0.00000000

B                 -2.78520300    3.68846700    0.00000000

B                 -2.64111600    0.77906500    1.17105100

B                  1.51095500    1.45392100    0.00000000

B                  1.17090800    2.92856600   -0.84211400

B                 -1.12319800    1.40940200   -0.88809400

B                 -0.41874700    2.87012900   -1.38737600

B                  0.57884900    1.44434500    1.45116400

B                  1.17090800    2.92856600    0.84211400

B                 -1.12319800    1.40940200    0.88809400

B                 -1.41058300    2.88076400    0.00000000

B                  0.57884900    1.44434500   -1.45116400

B                 -0.41874700    2.87012900    1.38737600

C                 -1.25222300   -6.43072300    0.00000000

C                 -4.37885200    3.03586800    0.00000000

B                  1.27930500    3.05604000    4.02666400

B                  4.11874800    3.08346800    0.00000000

B                  1.27930500    3.05604000   -4.02666400

B                 -3.40068000    3.01454000   -2.43441700

B                 -3.40068000    3.01454000    2.43441700

B                 -4.41728200    0.81131400   -1.34447000

B                 -4.41728200    0.81131400    1.34447000

C                 -4.25784300   -1.53916200    0.00000000

B                 -3.46286400   -1.53737800    2.51113800

C                 -3.87677000   -3.86689600    1.34629300

C                 -3.87677000   -3.86689600   -1.34629300

C                 -2.43166000   -3.79948600   -3.30103300

B                 -3.46286400   -1.53737800   -2.51113800

B                 -2.46570700    0.73803600   -3.47935300

B                 -0.06593200    0.74852600   -4.34356600

B                  2.77767800    0.85565500   -3.85267700

B                  1.30611600   -1.50423800   -4.04587600

C                  2.37381100   -3.82825300   -3.42160200

C                  4.03740600   -3.86268700   -1.22983400

C                 -2.43166000   -3.79948600    3.30103300

B                 -2.46570700    0.73803600    3.47935300

B                 -0.06593200    0.74852600    4.34356600

B                  2.77767800    0.85565500    3.85267700

B                  4.16594800    0.84886800    1.45419800

B                  4.16594800    0.84886800   -1.45419800

B                  4.46198700   -1.42703700    0.00000000

B                  1.30611600   -1.50423800    4.04587600

C                  2.37381100   -3.82825300    3.42160200

C                  4.03740600   -3.86268700    1.22983400

C                  1.21912800    6.40566100    0.00000000

B                 -2.17873500    5.70124000    1.56385700

B                  0.77088700    5.73921800    2.53394500

B                 -2.17873500    5.70124000   -1.56385700

B                  2.62072100    5.75661900    0.00000000

B                  0.77088700    5.73921800   -2.53394500

B                 -0.77882200   -5.73044300   -2.52476100

B                  2.15755800   -5.68375100   -1.55889700

B                  2.15755800   -5.68375100    1.55889700

B                 -2.64423200   -5.76703300    0.00000000

B                 -0.77882200   -5.73044300    2.52476100

B                  0.00502200   -3.85169500   -4.24359500

B                  0.00502200   -3.85169500    4.24359500

C                 -0.00218600    3.71302500    0.00000000

C                  0.07071600    0.69741300    0.00000000

C                  0.04377800   -0.74459800    0.00000000

C                  0.03012800   -3.73988600    0.00000000

C                 -2.19084600   -5.07826900   -2.56219200

C                 -2.19084600   -5.07826900    2.56219200

C                  0.33510800   -5.13778500   -3.42134900

C                  0.33510800   -5.13778500    3.42134900

C                  1.76044600   -5.09676200   -2.96313500

C                  1.76044600   -5.09676200    2.96313500

C                 -3.09390300   -5.12067300   -1.35304600

C                 -3.09390300   -5.12067300    1.35304600

C                  3.37058700   -5.08848100   -0.74476200

C                  3.37058700   -5.08848100    0.74476200

C                 -0.37323400   -6.42288400   -1.18921700

C                  1.02083300   -6.40207500   -0.73031300

C                  1.02083300   -6.40207500    0.73031300

C                 -0.37323400   -6.42288400    1.18921700

C                  0.34460500    6.39635900   -1.20214800

C                 -1.06343700    6.37820800   -0.74187300

C                 -1.06343700    6.37820800    0.74187300

C                  0.34460500    6.39635900    1.20214800

C                 -3.34011100    5.06710400   -0.74185500

C                 -3.34011100    5.06710400    0.74185500

C                 -1.77114400    5.05536100   -2.93087900

C                 -1.77114400    5.05536100    2.93087900

C                 -0.35752300    5.07038200   -3.40067400

C                 -0.35752300    5.07038200    3.40067400

C                  2.20838800    5.13558900   -2.56826800

C                  2.20838800    5.13558900    2.56826800

C                  3.09587200    5.13609100    1.36281500

C                  3.09587200    5.13609100   -1.36281500

C                 -3.96008600    3.79177400   -1.18809600

C                 -3.96008600    3.79177400    1.18809600

C                 -2.37564500    3.76667400   -3.36928400

C                 -2.37564500    3.76667400    3.36928400

C                 -0.11630900    3.79232400   -4.12995800

C                 -0.11630900    3.79232400    4.12995800

C                  3.84805800    3.84505600   -1.36928800

C                  3.84805800    3.84505600    1.36928800

C                  2.44326900    3.85766100   -3.29889800

C                  2.44326900    3.85766100    3.29889800

C                 -1.36174500    2.99954200   -4.11667100

C                 -1.36174500    2.99954200    4.11667100

C                  3.44487000    3.08865700   -2.57228000

C                  3.44487000    3.08865700    2.57228000

C                 -3.47751100    1.45424900   -2.42446400

C                 -3.47751100    1.45424900    2.42446400

C                 -1.37557900    1.53607400   -4.19063300

C                 -1.37557900    1.53607400    4.19063300

C                  1.36243300    1.49152500   -4.15211400

C                  1.36243300    1.49152500    4.15211400

C                 -4.60757500    1.60161500    0.00000000

C                  3.49827200    1.61977100   -2.67610600

C                  3.49827200    1.61977100    2.67610600

C                  4.23247700    1.53491500    0.00000000

C                 -4.12311200   -0.75235000   -1.25925600

C                 -4.12311200   -0.75235000    1.25925600

C                 -2.42621000   -0.87365900   -3.46667100

C                 -2.42621000   -0.87365900    3.46667100

C                 -0.11807600   -0.86818000   -4.24201400

C                 -0.11807600   -0.86818000    4.24201400

C                  2.53026000   -0.66941000   -3.39089200

C                  2.53026000   -0.66941000    3.39089200

C                  4.11145700   -0.70372900   -1.39086800

C                  4.11145700   -0.70372900    1.39086800

C                 -1.40112200   -1.68203200   -4.18258000

C                 -1.40112200   -1.68203200    4.18258000

C                  3.48343300   -1.50386200   -2.49532800

C                  3.48343300   -1.50386200    2.49532800

B                 -4.16758900   -3.11744700    0.00000000

B                  4.60194100   -3.09079700    0.00000000

C                 -3.47887700   -3.07957000   -2.54852200

C                 -3.47887700   -3.07957000    2.54852200

C                 -1.37969900   -3.12571700   -4.07838900

C                 -1.37969900   -3.12571700    4.07838900

C                  1.36561700   -3.05842000    4.16611100

C                  1.36561700   -3.05842000   -4.16611100

B                  3.42179100   -3.07690300   -2.47191800

B                  3.42179100   -3.07690300    2.47191800

Cs C88B78 (5)

B                 -2.53453500    0.73142100    1.81262100

B                  2.22397100    3.60041700   -1.62355200

B                  0.88534900    0.67110600   -2.85870900

B                  0.88534900    0.67110600    2.85870900

B                 -0.80939600    3.70106700    2.68816900

B                 -2.74965800    3.72097800    0.00000000

B                 -2.53453500    0.73142100   -1.81262100

B                 -0.80939600    3.70106700   -2.68816900

B                  0.05058300    5.33951600    0.00000000

B                  2.22397100    3.60041700    1.62355200

B                  2.82190300    0.51618300    0.00000000

B                 -1.27545100    1.35220700   -0.88777600

B                 -1.47520500    2.82151900    0.00000000

B                  0.40498500    1.35461800    1.42106100

B                 -0.49393600    2.83173800    1.39494700

B                  0.40498500    1.35461800   -1.42106100

B                 -0.49393600    2.83173800   -1.39494700

B                 -0.03496800    3.72463800    0.00000000

B                  1.44681700    1.39179800    0.00000000

B                  1.11411800    2.81371400    0.85068600

B                 -1.27545100    1.35220700    0.88777600

B                  1.11411800    2.81371400   -0.85068600

B                 -0.93810700   -1.22104100   -2.87524200

B                  0.82983800   -3.72499200    2.65077400

B                 -0.93810700   -1.22104100    2.87524200

B                  2.64232300   -0.88367700   -1.19372500

B                  0.82983800   -3.72499200   -2.65077400

B                 -2.29383700   -3.67422900   -1.63769000

B                 -3.02453400   -1.18103800    0.00000000

B                 -2.29383700   -3.67422900    1.63769000

B                 -0.06843800   -5.41257500    0.00000000

B                  2.76384100   -3.78274600    0.00000000

B                  2.64232300   -0.88367700    1.19372500

B                 -1.46517700   -1.52526200    0.00000000

B                 -1.15991300   -2.96107600   -0.84049400

B                  1.17987300   -1.52299200   -0.86243400

B                  0.43906400   -2.96023900   -1.35801900

B                 -0.44769800   -1.52462400    1.39609900

B                 -1.15991300   -2.96107600    0.84049400

B                 -0.01027100   -3.85365300    0.00000000

B                  1.17987300   -1.52299200    0.86243400

B                  1.42450900   -2.97566200    0.00000000

B                 -0.44769800   -1.52462400   -1.39609900

B                  0.43906400   -2.96023900    1.35801900

C                 -0.88095300    6.54857700   -0.73333600

C                 -0.88095300    6.54857700    0.73333600

C                  0.51674600    6.48149300    1.18178200

C                 -1.64380400    5.16109200    2.87919400

C                 -3.17991000    5.18627900    0.74337200

C                 -3.17991000    5.18627900   -0.74337200

C                 -1.64380400    5.16109200   -2.87919400

C                 -0.22320900    5.13493600   -3.35729200

C                  2.30279800    4.98792100   -2.53732800

C                  3.16347300    4.95841100   -1.30626100

C                  3.16347300    4.95841100    1.30626100

C                  2.30279800    4.98792100    2.53732800

C                 -0.22320900    5.13493600    3.35729200

B                 -1.34862700   -3.02284000    4.03816800

B                 -4.28410700   -2.97205000    0.00000000

B                 -1.34862700   -3.02284000   -4.03816800

B                  3.36028300   -3.11733100   -2.43592500

B                  3.36028300   -3.11733100    2.43592500

B                  4.43006300   -0.91256600   -1.32618900

B                  4.43006300   -0.91256600    1.32618900

B                  3.46019600    1.42608400    2.48600700

C                  3.50654300    2.94720100    2.49163000

C                  3.87625400    3.67095300    1.25142500

C                  3.87625400    3.67095300   -1.25142500

C                  3.50654300    2.94720100   -2.49163000

C                  2.50256200    3.72465900   -3.27696500

B                  3.46019600    1.42608400   -2.48600700

B                  2.49047800   -0.80286000   -3.49665100

B                  0.11290400   -0.70690600   -4.40793100

B                 -2.68975900   -0.65666300   -3.53152600

B                 -1.33127200    1.60636900   -4.07824400

C                  1.42179400    3.09225900   -4.06415300

C                 -1.36198400    3.14234600   -4.14232000

C                 -3.43146200    3.33864600   -2.50518500

C                 -2.35745300    3.94386400   -3.32049500

C                 -3.85054800    3.97699200   -1.24046500

C                 -3.43146200    3.33864600    2.50518500

C                 -1.36198400    3.14234600    4.14232000

C                  1.42179400    3.09225900    4.06415300

C                  2.50256200    3.72465900    3.27696500

B                  2.49047800   -0.80286000    3.49665100

B                  0.11290400   -0.70690600    4.40793100

B                 -2.68975900   -0.65666300    3.53152600

B                 -4.20577600   -0.62797800    1.45136100

B                 -4.20577600   -0.62797800   -1.45136100

B                 -4.31367700    1.65403300    0.00000000

B                 -1.33127200    1.60636900    4.07824400

C                 -2.35745300    3.94386400    3.32049500

C                 -3.85054800    3.97699200    1.24046500

B                  2.04286400   -5.80019600    1.55750100

B                 -0.91448200   -5.72302700    2.51823200

B                  2.04286400   -5.80019600   -1.55750100

B                 -2.74079600   -5.68185400    0.00000000

B                 -0.91448200   -5.72302700   -2.51823200

B                  0.90281600    5.70456100   -2.49125200

B                 -2.01393100    5.81349600   -1.53758300

B                 -2.01393100    5.81349600    1.53758300

B                  2.70962100    5.63756500    0.00000000

B                  0.90281600    5.70456100    2.49125200

B                  0.03417400    3.87144000   -4.21636000

B                  0.03417400    3.87144000    4.21636000

C                 -0.01366000   -0.76680600    0.00000000

C                 -0.05045500    0.65852900    0.00000000

C                  0.91540400   -6.53017700   -0.75010300

C                  0.91540400   -6.53017700    0.75010300

C                 -0.50842300   -6.48784500    1.20965200

C                 -0.50842300   -6.48784500   -1.20965200

C                  0.51674600    6.48149300   -1.18178200

C                 -4.30656100    3.21989700    0.00000000

C                 -1.38268100   -6.46370800    0.00000000

C                  3.24031100   -5.18589600   -0.74217700

C                  3.24031100   -5.18589600    0.74217700

C                  1.65975800   -5.12694300   -2.93309400

C                  1.65975800   -5.12694300    2.93309400

C                  0.23695800   -5.08809200   -3.39061800

C                  0.23695800   -5.08809200    3.39061800

C                 -2.33160400   -5.03909300   -2.56403400

C                 -2.33160400   -5.03909300    2.56403400

C                 -3.20898900   -5.02016300   -1.35063400

C                 -3.20898900   -5.02016300    1.35063400

C                  3.90914700   -3.92157000   -1.19252800

C                  3.90914700   -3.92157000    1.19252800

C                  2.30682700   -3.85020500   -3.37786600

C                  2.30682700   -3.85020500    3.37786600

C                  0.03000100   -3.80293500   -4.12289800

C                  0.03000100   -3.80293500    4.12289800

C                 -2.54224600   -3.74631000   -3.28774700

C                 -2.54224600   -3.74631000    3.28774700

C                 -3.94503300   -3.72268000   -1.34938600

C                 -3.94503300   -3.72268000    1.34938600

C                  1.30276900   -3.05446000   -4.12279200

C                  1.30276900   -3.05446000    4.12279200

C                 -3.54383400   -2.95153400   -2.54310100

C                 -3.54383400   -2.95153400    2.54310100

C                 -4.45949700   -1.40447300    0.00000000

C                  3.48338400   -1.54507200   -2.43110100

C                  3.48338400   -1.54507200    2.43110100

C                  1.35955000   -1.58507300   -4.20613800

C                  1.35955000   -1.58507300    4.20613800

C                 -1.38872600   -1.44932000   -4.22961600

C                 -1.38872600   -1.44932000    4.22961600

C                 -3.63030800   -1.48331600   -2.61602500

C                 -3.63030800   -1.48331600    2.61602500

C                  4.36694600   -3.17233000    0.00000000

C                  4.62922500   -1.73816800    0.00000000

C                  4.14737700    0.67141100   -1.24250400

C                  4.14737700    0.67141100    1.24250400

C                  2.42371300    0.79183500   -3.46817100

C                  2.42371300    0.79183500    3.46817100

C                  0.11403300    0.89531500   -4.28822300

C                  0.11403300    0.89531500    4.28822300

C                 -2.60821400    0.91184300   -3.45735300

C                 -2.60821400    0.91184300    3.45735300

C                 -4.12824200    0.95643400   -1.41322100

C                 -4.12824200    0.95643400    1.41322100

C                  4.17033600    2.97286000    0.00000000

C                  1.36817300    6.44527100    0.00000000

C                  4.28504200    1.48330100    0.00000000

C                  1.41585400    1.65647300   -4.18357300

C                  1.41585400    1.65647300    4.18357300

B                 -3.67029400    1.80777600   -2.66860400

B                 -3.67029400    1.80777600    2.66860400

Cs C88B78 (6)

B                  2.44124900   -0.74059300    1.76571200

B                 -2.21271100   -3.66686300   -1.61758500

B                 -0.90575800   -0.74731600   -2.85422100

B                 -0.90575800   -0.74731600    2.85422100

B                  0.79418100   -3.72310800    2.68074100

B                  2.72132500   -3.72554800    0.00000000

B                  2.44124900   -0.74059300   -1.76571200

B                  0.79418100   -3.72310800   -2.68074100

B                 -0.02485200   -5.35174500    0.00000000

B                 -2.21271100   -3.66686300    1.61758500

B                 -2.86373600   -0.58211300    0.00000000

B                 -0.00752600   -0.69065700    0.00000000

B                  1.21537700   -1.38326100   -0.87822000

B                  1.45216300   -2.84026000    0.00000000

B                 -0.44770800   -1.40438900    1.42361700

B                  0.47028400   -2.86349700    1.39732800

B                 -0.44770800   -1.40438900   -1.42361700

B                  0.47028400   -2.86349700   -1.39732800

B                  0.02735700   -3.74980000    0.00000000

B                 -1.49053900   -1.44494900    0.00000000

B                 -1.13432900   -2.86307000    0.84807100

B                  1.21537700   -1.38326100    0.87822000

B                 -1.13432900   -2.86307000   -0.84807100

B                  0.78302800    1.31442600   -2.89974200

B                 -0.82579700    3.78539700    2.64825000

B                  0.78302800    1.31442600    2.89974200

B                 -2.79901000    1.02026300   -0.96765600

B                 -0.82579700    3.78539700   -2.64825000

B                  2.28732300    3.68807000   -1.63759300

B                  2.95731700    1.25670800    0.00000000

B                  2.28732300    3.68807000    1.63759300

B                  0.09162500    5.44107900    0.00000000

B                 -2.72643900    3.88406700    0.00000000

B                 -2.79901000    1.02026300    0.96765600

B                 -0.08942800    0.81067000    0.00000000

B                  1.40302900    1.52948400    0.00000000

B                  1.15429100    2.97482700   -0.84623700

B                 -1.26136300    1.62397200   -0.85247300

B                 -0.45054200    3.02671300   -1.36059300

B                  0.37664700    1.56204400    1.40192200

B                  1.15429100    2.97482700    0.84623700

B                  0.03915900    3.89313300    0.00000000

B                 -1.26136300    1.62397200    0.85247300

B                 -1.40704300    3.08435200    0.00000000

B                  0.37664700    1.56204400   -1.40192200

B                 -0.45054200    3.02671300    1.36059300

C                 -0.46679600   -6.50083700   -1.18286600

C                  0.93203300   -6.54314100   -0.73231400

C                 -1.32236400   -6.47813600    0.00000000

C                  0.93203300   -6.54314100    0.73231400

C                 -0.46679600   -6.50083700    1.18286600

C                  3.94411400    3.72504000    1.34989700

C                  2.54269300    3.75182400   -3.29083300

C                 -2.30568600    3.85977200   -3.38652000

C                 -3.89249300    3.94215100    1.18985700

C                 -0.02806700    3.81585900    4.13017600

C                 -1.29725700    3.06225200   -4.11806200

C                 -4.27885100    3.18261700    0.00000000

C                 -1.29725700    3.06225200    4.11806200

C                  3.54357800    2.95920000    2.54699500

C                  3.54357800    2.95920000   -2.54699500

C                  1.68829200   -5.13737600    2.88678700

C                  3.22970200   -5.14113600    0.74796700

C                  3.22970200   -5.14113600   -0.74796700

C                  1.68829200   -5.13737600   -2.88678700

C                  0.26354900   -5.14956600   -3.37337900

C                 -2.27890600   -5.03577000   -2.54738400

C                 -3.14538700   -5.01762200   -1.31092200

C                 -3.14538700   -5.01762200    1.31092200

C                 -2.27890600   -5.03577000    2.54738400

C                  0.26354900   -5.14956600    3.37337900

C                  1.39171600    1.43204700   -4.22056300

C                 -3.51935200    1.53335100   -2.47343900

C                 -3.51935200    1.53335100    2.47343900

C                  1.39171600    1.43204700    4.22056300

C                  4.41254700    1.37845700    0.00000000

C                 -1.66764100    5.15690000    2.95577800

C                 -0.23845500    5.11785800    3.41334700

C                 -3.26276300    5.23312400    0.74948400

C                 -3.26276300    5.23312400   -0.74948400

C                  2.33609200    5.04966800    2.56977200

C                  3.21285400    5.02802200    1.35340500

C                 -1.66764100    5.15690000   -2.95577800

C                 -0.23845500    5.11785800   -3.41334700

C                  3.21285400    5.02802200   -1.35340500

C                  2.33609200    5.04966800   -2.56977200

B                  1.34980900    3.02522000    4.04248700

B                  4.27295600    2.96791300    0.00000000

B                  1.34980900    3.02522000   -4.04248700

B                 -3.36525700    3.11555700   -2.44573900

B                 -3.36525700    3.11555700    2.44573900

B                 -4.43500100    0.85563600   -1.39898300

B                 -4.43500100    0.85563600    1.39898300

C                 -4.17620400   -0.72053200   -1.25562900

C                 -4.17620400   -0.72053200    1.25562900

C                 -4.32384900   -1.52247700    0.00000000

B                 -3.46038700   -1.46275400    2.48343600

C                 -4.16036200   -3.02193500    0.00000000

C                 -3.49045900   -2.99400900    2.49173200

C                 -3.86437000   -3.72415000    1.25343000

C                 -3.86437000   -3.72415000   -1.25343000

C                 -3.49045900   -2.99400900   -2.49173200

C                 -2.49005500   -3.76133300   -3.28043400

B                 -3.46038700   -1.46275400   -2.48343600

C                 -2.43172100   -0.81045000   -3.47565100

B                 -2.50175700    0.79745000   -3.49810800

B                 -0.11371800    0.70378500   -4.43321200

B                  2.66456100    0.66717200   -3.50542800

C                  2.59645300   -0.93181600   -3.39354500

C                  3.56378800   -1.77277600   -2.59180800

B                  1.31495100   -1.60581100   -4.06233000

C                 -0.11770800   -0.89967900   -4.29026600

C                 -1.42329100   -1.67261000   -4.20603500

C                 -1.41783100   -3.11322500   -4.07410500

C                  1.35970100   -3.13168500   -4.13864300

C                  3.39035500   -3.21824400   -2.47406300

C                  4.29338200   -3.16853700    0.00000000

C                  2.35420500   -3.88582400   -3.31952600

C                  3.85259900   -3.89878000   -1.22908100

C                  3.39035500   -3.21824400    2.47406300

C                  1.35970100   -3.13168500    4.13864300

C                 -1.41783100   -3.11322500    4.07410500

C                 -2.49005500   -3.76133300    3.28043400

B                 -2.50175700    0.79745000    3.49810800

C                 -2.43172100   -0.81045000    3.47565100

C                 -1.42329100   -1.67261000    4.20603500

B                 -0.11371800    0.70378500    4.43321200

C                 -0.11770800   -0.89967900    4.29026600

B                  2.66456100    0.66717200    3.50542800

C                  2.59645300   -0.93181600    3.39354500

B                  4.15653600    0.63695800    1.45671400

C                  4.05097500   -0.96558700    1.42279000

B                  4.15653600    0.63695800   -1.45671400

C                  4.05097500   -0.96558700   -1.42279000

B                  4.26678600   -1.63633300    0.00000000

C                  3.56378800   -1.77277600    2.59180800

B                  1.31495100   -1.60581100    4.06233000

C                  2.35420500   -3.88582400    3.31952600

C                  3.85259900   -3.89878000    1.22908100

C                 -0.90961700    6.55274800    0.75116100

C                  0.51403500    6.51460800    1.21167700

C                 -0.90961700    6.55274800   -0.75116100

C                  1.39130100    6.49420900    0.00000000

C                  0.51403500    6.51460800   -1.21167700

B                 -2.04623600    5.82934500    1.56907000

B                  0.91658400    5.73957000    2.52605000

B                 -2.04623600    5.82934500   -1.56907000

B                  2.74441700    5.69257300    0.00000000

B                  0.91658400    5.73957000   -2.52605000

C                  3.94411400    3.72504000   -1.34989700

C                  2.54269300    3.75182400    3.29083300

C                 -2.30568600    3.85977200    3.38652000

C                 -0.02806700    3.81585900   -4.13017600

C                 -3.89249300    3.94215100   -1.18985700

C                  3.62413200    1.48870200    2.61933800

C                  3.62413200    1.48870200   -2.61933800

C                 -1.34935900    1.58263200   -4.19811000

C                 -4.36592900    1.68538700    0.00000000

C                 -1.34935900    1.58263200    4.19811000

B                 -0.86563000   -5.72989400   -2.49855500

B                  2.05645100   -5.78339200   -1.53819300

B                  2.05645100   -5.78339200    1.53819300

B                 -2.68234000   -5.68754100    0.00000000

B                 -0.86563000   -5.72989400    2.49855500

B                 -0.02664500   -3.88325900   -4.22268800

B                 -0.02664500   -3.88325900    4.22268800

Cs B180 (7)

B                 -0.89190900    1.10069300    3.52493500

B                  0.82802000    1.12036800    3.56590000

B                  1.37029700   -0.50752000    3.58774400

B                 -1.41410400   -0.54281100    3.55579700

B                 -0.00503400   -1.52676000    3.58510300

B                  1.45401000    0.41340100    2.05248400

B                  0.94482100   -1.29105800    2.05448500

B                 -1.44575200    0.35418500    2.01980100

B                 -0.82229500   -1.31837900    2.05827900

B                 -0.03240500   -0.05907400    4.50429700

B                  0.03308300   -0.08319500    0.95212400

B                 -1.73987100    3.83176100    4.04018100

B                 -3.19993100    2.77899300    3.97368600

B                 -3.20138700    1.93906100    5.49949000

B                 -1.75801400    2.35909200    6.39260700

B                 -0.90297100    3.48451800    5.50055600

B                  0.75027200    1.13070700    7.30807200

B                 -1.50961400   -0.50458000    7.30343200

B                 -3.74809200    0.31997300    5.50690200

B                 -2.88207700   -0.91384100    6.40026400

B                 -0.12481800   -1.51245700    7.24900300

B                 -1.52191700   -3.40438700    5.49462900

B                 -4.32704300   -0.37684100    4.08960600

B                 -1.91365100   -3.71653100    2.75627100

B                 -3.49588600   -2.88371700    2.66820800

B                 -1.40503500   -2.82861300    0.00000000

B                 -3.87333400   -2.11223500    1.28706400

B                 -2.83122500   -1.81038900    0.00000000

B                 -4.40197600   -0.38353000    1.18592600

B                 -4.53200300    0.52871800    2.57043400

B                 -3.93328500    2.14160300    2.57194600

B                 -3.11966200    2.74013600    1.21815400

B                 -3.19837800   -0.08722000    0.00000000

B                 -2.96503200    1.64075900    0.00000000

B                 -0.74075200   -3.43157000    1.42879600

B                 -0.98072300   -4.23461900    4.05121900

B                  0.86935900   -3.92529000    1.31687900

B                  1.85577600   -4.07112500    2.69529200

B                  1.81089900   -3.59032500    0.00000000

B                 -0.63778200    3.82328500    0.00000000

B                 -1.69606000    3.71624700    1.25318600

B                 -0.83524300    4.31647600    2.65063300

B                  0.95226300    3.84848800    0.00000000

B                  3.21217000   -2.80285200    0.00000000

B                  3.68829800   -2.10997400    1.49476100

B                  4.15995500   -0.49514800    1.48148200

B                  4.09800400    0.37810300    0.00000000

B                  3.62728200    1.93920400    0.00000000

B                  3.15489900    2.68905300    1.46808900

B                  1.77876200    3.65485700    1.47629800

B                  3.94417000    2.09780500    2.80164600

B                  4.44831800    0.46744800    2.80973200

B                  4.17322600   -0.53090900    4.21466000

B                  3.61680100   -2.18023600    4.20238100

B                  3.27655900   -3.10469100    2.78466700

B                  1.27741100   -3.46718300    5.56085300

B                  2.67537400   -2.42398300    5.62284200

B                  2.60745500   -0.94922600    6.48316000

B                  1.27465500   -0.50826900    7.34662900

B                 -0.14855800   -2.92330500    6.37929300

B                  3.56894600    0.19710000    5.65291000

B                  1.59009500    2.25379300    6.45141400

B                  3.03382200    1.84745500    5.63676700

B                  3.12417500    2.76857600    4.18387300

B                  0.82102100    3.49269900    5.56904700

B                  0.88861000    4.29771400    2.71340600

B                  1.72170000    3.79172300    4.14187600

B                  0.79054600   -4.20777700    4.08609800

B                 -0.10408400   -0.03048300    6.21420000

B                 -3.91841100   -2.08634300    4.12300500

B                 -2.85612700   -2.37118500    5.47754000

B                 -0.11357700   -2.80024400    4.60524700

B                 -2.11985200   -2.54951800    1.48692400

B                 -2.68484800   -0.85806000    4.58992500

B                 -2.95602600    0.88073800    1.51775800

B                 -1.67053000    2.13354900    4.57402500

B                 -0.00763000    3.04977100    1.43923300

B                  1.54985200    2.12727400    4.68056500

B                  3.00062500    0.89660500    1.50862800

B                  2.51478300   -0.89503600    4.72397100

B                  1.94062200   -2.55143100    1.48764700

B                 -0.09987700   -0.07199100    8.14506400

B                  4.08449200   -1.44519300    5.67185100

B                  2.52932000    3.48470200    5.62520400

B                 -2.64731300    3.53394400    5.42590300

B                 -4.27917500   -1.32753800    5.56051900

B                 -0.16421200   -4.42918700    5.51741800

B                 -0.00687200    1.44288600    2.02239000

B                 -0.89190900    1.10069300   -3.52493500

B                 -1.41410400   -0.54281100   -3.55579700

B                 -0.00503400   -1.52676000   -3.58510300

B                  0.82802000    1.12036800   -3.56590000

B                  1.37029700   -0.50752000   -3.58774400

B                 -0.82229500   -1.31837900   -2.05827900

B                  0.94482100   -1.29105800   -2.05448500

B                 -0.00687200    1.44288600   -2.02239000

B                  1.45401000    0.41340100   -2.05248400

B                 -0.03240500   -0.05907400   -4.50429700

B                  0.03308300   -0.08319500   -0.95212400

B                 -3.19993100    2.77899300   -3.97368600

B                 -1.73987100    3.83176100   -4.04018100

B                 -0.90297100    3.48451800   -5.50055600

B                 -1.75801400    2.35909200   -6.39260700

B                 -3.20138700    1.93906100   -5.49949000

B                 -0.94284600    1.17906000   -7.32652800

B                 -1.50961400   -0.50458000   -7.30343200

B                  0.75027200    1.13070700   -7.30807200

B                  0.82102100    3.49269900   -5.56904700

B                  1.59009500    2.25379300   -6.45141400

B                  1.27465500   -0.50826900   -7.34662900

B                  3.56894600    0.19710000   -5.65291000

B                  1.72170000    3.79172300   -4.14187600

B                  4.44831800    0.46744800   -2.80973200

B                  3.94417000    2.09780500   -2.80164600

B                  3.15489900    2.68905300   -1.46808900

B                  1.77876200    3.65485700   -1.47629800

B                  0.88861000    4.29771400   -2.71340600

B                 -0.83524300    4.31647600   -2.65063300

B                 -1.69606000    3.71624700   -1.25318600

B                  4.15995500   -0.49514800   -1.48148200

B                  4.17322600   -0.53090900   -4.21466000

B                  3.68829800   -2.10997400   -1.49476100

B                  3.27655900   -3.10469100   -2.78466700

B                 -3.11966200    2.74013600   -1.21815400

B                 -3.93328500    2.14160300   -2.57194600

B                  0.86935900   -3.92529000   -1.31687900

B                 -0.74075200   -3.43157000   -1.42879600

B                 -3.87333400   -2.11223500   -1.28706400

B                 -4.40197600   -0.38353000   -1.18592600

B                 -3.49588600   -2.88371700   -2.66820800

B                 -1.91365100   -3.71653100   -2.75627100

B                 -0.98072300   -4.23461900   -4.05121900

B                  0.79054600   -4.20777700   -4.08609800

B                  1.85577600   -4.07112500   -2.69529200

B                  2.67537400   -2.42398300   -5.62284200

B                  1.27741100   -3.46718300   -5.56085300

B                 -0.14855800   -2.92330500   -6.37929300

B                 -0.12481800   -1.51245700   -7.24900300

B                  2.60745500   -0.94922600   -6.48316000

B                 -1.52191700   -3.40438700   -5.49462900

B                 -2.88207700   -0.91384100   -6.40026400

B                 -2.85612700   -2.37118500   -5.47754000

B                 -3.91841100   -2.08634300   -4.12300500

B                 -3.74809200    0.31997300   -5.50690200

B                 -4.53200300    0.52871800   -2.57043400

B                 -4.32704300   -0.37684100   -4.08960600

B                  3.61680100   -2.18023600   -4.20238100

B                 -0.10408400   -0.03048300   -6.21420000

B                  3.12417500    2.76857600   -4.18387300

B                  3.03382200    1.84745500   -5.63676700

B                  2.51478300   -0.89503600   -4.72397100

B                  3.00062500    0.89660500   -1.50862800

B                  1.54985200    2.12727400   -4.68056500

B                 -0.00763000    3.04977100   -1.43923300

B                 -1.67053000    2.13354900   -4.57402500

B                 -2.95602600    0.88073800   -1.51775800

B                 -2.68484800   -0.85806000   -4.58992500

B                 -2.11985200   -2.54951800   -1.48692400

B                 -0.11357700   -2.80024400   -4.60524700

B                  1.94062200   -2.55143100   -1.48764700

B                 -0.09987700   -0.07199100   -8.14506400

B                 -0.16421200   -4.42918700   -5.51741800

B                 -4.27917500   -1.32753800   -5.56051900

B                 -2.64731300    3.53394400   -5.42590300

B                  2.52932000    3.48470200   -5.62520400

B                  4.08449200   -1.44519300   -5.67185100

B                 -1.44575200    0.35418500   -2.01980100

B                 -0.94284600    1.17906000    7.32652800

B                 -2.24830400    0.70837600    6.32787400

B                 -0.01142100    4.17411200    4.05952100

B                  2.39264200   -3.49827600    4.12687500

B                  3.96382200    1.21106300    4.18911600

B                 -4.31596700   -1.26625200    2.60998000

B                  4.09127400   -1.39168400    0.00000000

B                  2.54325100    3.33069600    0.00000000

B                 -4.31596700   -1.26625200   -2.60998000

B                  2.39264200   -3.49827600   -4.12687500

B                  3.96382200    1.21106300   -4.18911600

B                 -0.01142100    4.17411200   -4.05952100

B                 -2.24830400    0.70837600   -6.32787400

Cs B182 (8)

B                 -1.42342200   -0.08552400    3.61659300

B                 -0.43677900    1.32829300    3.62442100

B                  1.21473900    0.85757800    3.55961700

B                 -0.40491400   -1.46885400    3.52296800

B                  1.25020200   -0.88272200    3.44741900

B                  0.41681200    1.45144600    2.04525700

B                  1.48033500    0.05825100    1.97119200

B                 -1.22998400   -0.91337100    2.02994900

B                  0.44698600   -1.41678400    1.96067700

B                  0.07393300   -0.08159800    4.52186700

B                 -0.04197800    0.01913700    0.94595200

B                 -4.18219100    0.79036100    4.29896600

B                 -4.16667500   -1.00624800    4.29245900

B                 -3.27640100   -1.51645200    5.64673300

B                 -2.81125900   -0.12775700    6.52265800

B                 -3.31683600    1.27778200    5.68455400

B                 -0.39995200    1.30432300    7.36115200

B                 -0.39199000   -1.48142300    7.34958900

B                 -2.30154400   -2.87135900    5.54951900

B                 -0.81564300   -2.84441900    6.40729700

B                  1.28349700   -0.92032200    7.36447900

B                  2.01910700   -3.09036200    5.50500200

B                 -2.11928900   -3.84489400    4.14574600

B                  2.28948400   -3.80910600    2.70556200

B                  0.56853600   -4.26337600    2.76750000

B                  1.78554800   -2.66052000    0.00000000

B                 -0.47244200   -4.03653500    1.41006600

B                  0.33918200   -3.69472500    0.00000000

B                 -2.17836000   -3.63584600    1.45199400

B                 -3.03955000   -3.30483000    2.80940400

B                 -4.06080900   -1.90307100    2.80824600

B                 -4.19082200   -0.97281500    1.44262400

B                 -2.86059100   -3.04981800    0.00000000

B                 -3.80797700   -1.72964400    0.00000000

B                  2.89263700   -3.05277100    1.43504600

B                  3.01057400   -3.19760700    4.13010300

B                  3.89634400   -1.54487700    1.45371300

B                  4.48508400   -0.74560400    2.72262400

B                  3.17206500   -0.68642000    0.00000000

B                 -3.76489300    1.62286400    0.00000000

B                 -4.16172600    0.85977200    1.45701400

B                 -4.06685200    1.75357000    2.83915000

B                 -2.83024700    2.94917100    0.00000000

B                  3.52960900    1.01942800    0.00000000

B                  3.79913300    1.83459600    1.37575200

B                  2.69217200    3.25859400    1.37527600

B                  1.83837500    3.58967300    0.00000000

B                  0.29835400    4.06789100    0.00000000

B                 -0.52866000    4.22560000    1.45288100

B                 -2.25869700    3.58789300    1.45934800

B                  0.39424200    4.41334000    2.80583600

B                  2.08571100    3.91843100    2.77322100

B                  2.80571200    3.26170200    4.23319700

B                  3.93745600    1.86773700    4.18096600

B                  4.33965200    1.03698900    2.70905600

B                  3.59021400   -0.76769400    5.52248800

B                  3.58047600    0.89899200    5.55800300

B                  2.35958800    1.67057000    6.45810300

B                  1.24892700    0.79839500    7.30493800

B                  2.44869200   -1.68187200    6.42063600

B                  1.85761800    3.08689200    5.63676700

B                 -0.88384400    2.63979800    6.52905900

B                  0.26515700    3.56815500    5.66001200

B                 -0.49385100    4.21307800    4.29307800

B                 -2.37394300    2.64435900    5.68110900

B                 -3.06763900    3.19011100    2.83338500

B                 -2.20232400    3.61741400    4.29756900

B                  4.08190500   -1.66886100    4.13543900

B                  0.08837000   -0.11000100    6.23500900

B                 -0.38445600   -4.39459500    4.12683400

B                  0.39227400   -3.70726600    5.52027000

B                  2.32215600   -1.56513500    4.58696700

B                  0.95788300   -3.01338900    1.49992600

B                 -0.77082800   -2.73722300    4.51903400

B                 -2.52381700   -1.90737900    1.63244200

B                 -2.68168200   -0.10565400    4.72226600

B                 -2.55080200    1.76079400    1.67854100

B                 -0.85175900    2.51426800    4.73038800

B                  0.92865800    2.96770600    1.56874600

B                  2.23157100    1.62125100    4.64508300

B                  3.11380800    0.19808100    1.51484100

B                  0.07023000   -0.03913200    8.16556000

B                  3.49491800    2.60022200    5.65863000

B                 -1.37680000    4.02537000    5.75057300

B                 -4.28289800   -0.13027400    5.74577800

B                 -1.28684700   -4.24658300    5.52255400

B                  3.66521900   -2.50426300    5.52794200

B                 -1.23206600    0.84366300    2.07815800

B                 -1.42342200   -0.08552400   -3.61659300

B                 -0.40491400   -1.46885400   -3.52296800

B                  1.25020200   -0.88272200   -3.44741900

B                 -0.43677900    1.32829300   -3.62442100

B                  1.21473900    0.85757800   -3.55961700

B                  0.44698600   -1.41678400   -1.96067700

B                  1.48033500    0.05825100   -1.97119200

B                 -1.23206600    0.84366300   -2.07815800

B                  0.41681200    1.45144600   -2.04525700

B                  0.07393300   -0.08159800   -4.52186700

B                 -0.04197800    0.01913700   -0.94595200

B                 -4.16667500   -1.00624800   -4.29245900

B                 -4.18219100    0.79036100   -4.29896600

B                 -3.31683600    1.27778200   -5.68455400

B                 -2.81125900   -0.12775700   -6.52265800

B                 -3.27640100   -1.51645200   -5.64673300

B                 -1.38546100   -0.11215900   -7.33236700

B                 -0.39199000   -1.48142300   -7.34958900

B                 -0.39995200    1.30432300   -7.36115200

B                 -2.37394300    2.64435900   -5.68110900

B                 -0.88384400    2.63979800   -6.52905900

B                  1.24892700    0.79839500   -7.30493800

B                  1.85761800    3.08689200   -5.63676700

B                 -2.20232400    3.61741400   -4.29756900

B                  2.08571100    3.91843100   -2.77322100

B                  0.39424200    4.41334000   -2.80583600

B                 -0.52866000    4.22560000   -1.45288100

B                 -2.25869700    3.58789300   -1.45934800

B                 -3.06763900    3.19011100   -2.83338500

B                 -4.06685200    1.75357000   -2.83915000

B                 -4.16172600    0.85977200   -1.45701400

B                  2.69217200    3.25859400   -1.37527600

B                  2.80571200    3.26170200   -4.23319700

B                  3.79913300    1.83459600   -1.37575200

B                  4.33965200    1.03698900   -2.70905600

B                 -4.19082200   -0.97281500   -1.44262400

B                 -4.06080900   -1.90307100   -2.80824600

B                  3.89634400   -1.54487700   -1.45371300

B                  2.89263700   -3.05277100   -1.43504600

B                 -0.47244200   -4.03653500   -1.41006600

B                 -2.17836000   -3.63584600   -1.45199400

B                  0.56853600   -4.26337600   -2.76750000

B                  2.28948400   -3.80910600   -2.70556200

B                  3.01057400   -3.19760700   -4.13010300

B                  4.08190500   -1.66886100   -4.13543900

B                  4.48508400   -0.74560400   -2.72262400

B                  3.58047600    0.89899200   -5.55800300

B                  3.59021400   -0.76769400   -5.52248800

B                  2.44869200   -1.68187200   -6.42063600

B                  1.28349700   -0.92032200   -7.36447900

B                  2.35958800    1.67057000   -6.45810300

B                  2.01910700   -3.09036200   -5.50500200

B                 -0.81564300   -2.84441900   -6.40729700

B                  0.39227400   -3.70726600   -5.52027000

B                 -0.38445600   -4.39459500   -4.12683400

B                 -2.30154400   -2.87135900   -5.54951900

B                 -3.03955000   -3.30483000   -2.80940400

B                 -2.11928900   -3.84489400   -4.14574600

B                  3.93745600    1.86773700   -4.18096600

B                  0.08837000   -0.11000100   -6.23500900

B                 -0.49385100    4.21307800   -4.29307800

B                  0.26515700    3.56815500   -5.66001200

B                  2.23157100    1.62125100   -4.64508300

B                  0.92865800    2.96770600   -1.56874600

B                 -0.85175900    2.51426800   -4.73038800

B                 -2.55080200    1.76079400   -1.67854100

B                 -2.68168200   -0.10565400   -4.72226600

B                 -2.52381700   -1.90737900   -1.63244200

B                 -0.77082800   -2.73722300   -4.51903400

B                  0.95788300   -3.01338900   -1.49992600

B                  2.32215600   -1.56513500   -4.58696700

B                  3.11380800    0.19808100   -1.51484100

B                  0.07023000   -0.03913200   -8.16556000

B                  3.66521900   -2.50426300   -5.52794200

B                 -1.28684700   -4.24658300   -5.52255400

B                 -4.28289800   -0.13027400   -5.74577800

B                 -1.37680000    4.02537000   -5.75057300

B                  3.49491800    2.60022200   -5.65863000

B                 -1.22998400   -0.91337100   -2.02994900

B                 -1.38546100   -0.11215900    7.33236700

B                  0.79877000   -2.33848900    6.52065300

B                 -1.36578700    3.99341900    2.88594100

B                 -4.26464000   -0.12310200    2.88350100

B                  2.81209400   -1.95083200    2.88602900

B                  3.40424100    2.69513300    2.76025800

B                 -1.35018400    3.81127000    0.00000000

B                 -4.04680500   -0.07268800    0.00000000

B                 -1.39873000   -3.89907800    0.00000000

B                  3.41849100   -2.32867300    0.00000000

B                  2.81209400   -1.95083200   -2.88602900

B                  3.40424100    2.69513300   -2.76025800

B                 -1.36578700    3.99341900   -2.88594100

B                 -4.26464000   -0.12310200   -2.88350100

B                  0.79877000   -2.33848900   -6.52065300

Cs B184 (9)

B                 -1.07928000    0.98496400    3.58414200

B                  0.60438400    1.29395000    3.59779600

B                  1.40955400   -0.21459800    3.60996900

B                 -1.30728400   -0.72162000    3.57589000

B                  0.23728600   -1.45882900    3.58361700

B                  1.26532200    0.69690900    2.05045700

B                  1.04193600   -1.06250100    2.03969300

B                 -1.56688200    0.18506600    2.07149800

B                 -0.71644600   -1.39349400    2.03179500

B                 -0.02918100   -0.02451100    4.55513600

B                 -0.14106700   -0.00838400    0.94834900

B                 -2.43213800    3.46270200    4.16422400

B                 -3.62253000    2.21160400    4.16540000

B                 -3.41526500    1.29672100    5.61303000

B                 -2.06656800    1.91400400    6.47137600

B                 -1.51649500    3.29973600    5.61700500

B                  0.60648500    1.26694200    7.36401000

B                 -1.29614800   -0.74062100    7.34780600

B                 -3.63992000   -0.42569500    5.60736300

B                 -2.50772500   -1.39326800    6.45684300

B                  0.24874300   -1.47878400    7.34063400

B                 -0.76033600   -3.60240100    5.55498100

B                 -4.09137600   -1.23166400    4.15402100

B                 -1.13816300   -4.30572400    2.68242300

B                 -2.70772300   -3.58274600    2.71904800

B                 -1.10135800   -3.80344400    0.00000000

B                 -3.24191000   -2.66410800    1.46760600

B                 -2.61363000   -3.23477300    0.00000000

B                 -4.02467300   -1.15370000    1.45594300

B                 -4.51896600   -0.26890900    2.76646000

B                 -4.27533400    1.42632200    2.76685200

B                 -3.57923900    2.15961300    1.46284100

B                 -4.10208400   -0.26767300    0.00000000

B                 -3.94641200    1.37638000    0.00000000

B                 -0.11892400   -4.09313800    1.29306900

B                 -0.12289900   -4.22918600    4.07776100

B                  1.56858000   -3.75935900    1.28846400

B                  2.56156200   -3.60182400    2.69110200

B                  2.45397300   -3.16798300    0.00000000

B                 -1.55634900    3.73665200    0.00000000

B                 -2.35628100    3.37447500    1.45501000

B                 -1.65755900    4.13305100    2.75815600

B                  0.07743800    4.07693100    0.00000000

B                  3.78740500   -2.18945000    0.00000000

B                  3.99922200   -1.37558600    1.46538800

B                  4.20578500    0.34879700    1.45704300

B                  4.14499200    1.21019200    0.00000000

B                  3.13933700    2.56036700    0.00000000

B                  2.46435500    3.15623000    1.44880900

B                  0.93473600    3.95883300    1.45816300

B                  3.40545500    2.80207900    2.76958300

B                  4.25654800    1.33729800    2.78078900

B                  4.22441800    0.30081700    4.17442800

B                  3.97893300   -1.40703800    4.15539800

B                  3.75775700   -2.38680200    2.75407400

B                  1.95594000   -3.10606500    5.56593700

B                  3.14276500   -1.83896900    5.59914000

B                  2.78422100   -0.40568200    6.47425100

B                  1.42011900   -0.23365100    7.35947800

B                  0.50067600   -2.82836000    6.43274100

B                  3.50831400    0.90217700    5.62843400

B                  1.19598700    2.51338500    6.47595300

B                  2.68009300    2.42848900    5.62825600

B                  2.55163400    3.35451100    4.17209200

B                  0.18604000    3.61421900    5.61653800

B                  0.02864000    4.43063200    2.75583500

B                  0.98342900    4.08306800    4.16049000

B                  1.58633000   -3.93727600    4.08872900

B                 -0.01357700   -0.03748300    6.27577100

B                 -3.25612800   -2.74996600    4.13372300

B                 -2.32967200   -2.85768800    5.57644800

B                  0.49169300   -2.68134100    4.65767600

B                 -1.39980900   -2.84163500    1.47741500

B                 -2.40200700   -1.31697100    4.67699100

B                 -3.16063300    0.41865300    1.54705700

B                 -1.97951400    1.84162300    4.69007000

B                 -0.59744700    3.06362100    1.55864700

B                  1.15499200    2.41322300    4.68822100

B                  2.79257600    1.41709800    1.52491700

B                  2.67033900   -0.36324400    4.67539100

B                  2.32989600   -2.16331800    1.48562000

B                 -0.02458500   -0.05398800    8.19641500

B                  4.31353800   -0.60476700    5.63011400

B                  1.85565000    3.92389200    5.63418400

B                 -3.19277300    2.98720100    5.63533000

B                 -3.86953200   -2.12057700    5.60978300

B                  0.77076200   -4.34410600    5.54363400

B                 -0.32677100    1.47033800    2.04090500

B                 -1.07928000    0.98496400   -3.58414200

B                 -1.30728400   -0.72162000   -3.57589000

B                  0.23728600   -1.45882900   -3.58361700

B                  0.60438400    1.29395000   -3.59779600

B                  1.40955400   -0.21459800   -3.60996900

B                 -0.71644600   -1.39349400   -2.03179500

B                  1.04193600   -1.06250100   -2.03969300

B                 -0.32677100    1.47033800   -2.04090500

B                  1.26532200    0.69690900   -2.05045700

B                 -0.02918100   -0.02451100   -4.55513600

B                 -0.14106700   -0.00838400   -0.94834900

B                 -3.62253000    2.21160400   -4.16540000

B                 -2.43213800    3.46270200   -4.16422400

B                 -1.51649500    3.29973600   -5.61700500

B                 -2.06656800    1.91400400   -6.47137600

B                 -3.41526500    1.29672100   -5.61303000

B                 -1.07220700    0.95711100   -7.35887900

B                 -1.29614800   -0.74062100   -7.34780600

B                  0.60648500    1.26694200   -7.36401000

B                  0.18604000    3.61421900   -5.61653800

B                  1.19598700    2.51338500   -6.47595300

B                  1.42011900   -0.23365100   -7.35947800

B                  3.50831400    0.90217700   -5.62843400

B                  0.98342900    4.08306800   -4.16049000

B                  4.25654800    1.33729800   -2.78078900

B                  3.40545500    2.80207900   -2.76958300

B                  2.46435500    3.15623000   -1.44880900

B                  0.93473600    3.95883300   -1.45816300

B                  0.02864000    4.43063200   -2.75583500

B                 -1.65755900    4.13305100   -2.75815600

B                 -2.35628100    3.37447500   -1.45501000

B                  4.20578500    0.34879700   -1.45704300

B                  4.22441800    0.30081700   -4.17442800

B                  3.99922200   -1.37558600   -1.46538800

B                  3.75775700   -2.38680200   -2.75407400

B                 -3.57923900    2.15961300   -1.46284100

B                 -4.27533400    1.42632200   -2.76685200

B                  1.56858000   -3.75935900   -1.28846400

B                 -0.11892400   -4.09313800   -1.29306900

B                 -3.24191000   -2.66410800   -1.46760600

B                 -4.02467300   -1.15370000   -1.45594300

B                 -2.70772300   -3.58274600   -2.71904800

B                 -1.13816300   -4.30572400   -2.68242300

B                 -0.12289900   -4.22918600   -4.07776100

B                  1.58633000   -3.93727600   -4.08872900

B                  2.56156200   -3.60182400   -2.69110200

B                  3.14276500   -1.83896900   -5.59914000

B                  1.95594000   -3.10606500   -5.56593700

B                  0.50067600   -2.82836000   -6.43274100

B                  0.24874300   -1.47878400   -7.34063400

B                  2.78422100   -0.40568200   -6.47425100

B                 -0.76033600   -3.60240100   -5.55498100

B                 -2.50772500   -1.39326800   -6.45684300

B                 -2.32967200   -2.85768800   -5.57644800

B                 -3.25612800   -2.74996600   -4.13372300

B                 -3.63992000   -0.42569500   -5.60736300

B                 -4.51896600   -0.26890900   -2.76646000

B                 -4.09137600   -1.23166400   -4.15402100

B                  3.97893300   -1.40703800   -4.15539800

B                 -0.01357700   -0.03748300   -6.27577100

B                  2.55163400    3.35451100   -4.17209200

B                  2.68009300    2.42848900   -5.62825600

B                  2.67033900   -0.36324400   -4.67539100

B                  2.79257600    1.41709800   -1.52491700

B                  1.15499200    2.41322300   -4.68822100

B                 -0.59744700    3.06362100   -1.55864700

B                 -1.97951400    1.84162300   -4.69007000

B                 -3.16063300    0.41865300   -1.54705700

B                 -2.40200700   -1.31697100   -4.67699100

B                 -1.39980900   -2.84163500   -1.47741500

B                  0.49169300   -2.68134100   -4.65767600

B                  2.32989600   -2.16331800   -1.48562000

B                 -0.02458500   -0.05398800   -8.19641500

B                  0.77076200   -4.34410600   -5.54363400

B                 -3.86953200   -2.12057700   -5.60978300

B                 -3.19277300    2.98720100   -5.63533000

B                  1.85565000    3.92389200   -5.63418400

B                  4.31353800   -0.60476700   -5.63011400

B                 -1.56688200    0.18506600   -2.07149800

B                 -1.07220700    0.95711100    7.35887900

B                 -0.78893800    4.08371400    4.15437300

B                 -4.18002900    0.52916600    4.15825900

B                 -1.84736000   -3.83074300    4.08599900

B                  3.00497700   -2.90016200    4.12523700

B                  3.62559700    1.95522000    4.18608100

B                  4.41339900   -0.61556900    0.00000000

B                  1.73855900    3.74501300    0.00000000

B                 -3.09869700    2.85651700    0.00000000

B                 -3.76122600   -2.03233800    0.00000000

B                 -4.18002900    0.52916600   -4.15825900

B                 -1.84736000   -3.83074300   -4.08599900

B                  3.00497700   -2.90016200   -4.12523700

B                  3.62559700    1.95522000   -4.18608100

B                 -0.78893800    4.08371400   -4.15437300

B                  2.27835300   -0.32239000   -0.90866000

B                  2.27835300   -0.32239000    0.90866000