Electronic Supporting Material

Efficient thin-film micro extraction of trace herbicides from food samples using composite electrospun PVC/EVA/CS/Str nanofibers prior to CD-IMS analysis

Fatemeh Nejabatia, Shima Aminia, Homeira Ebrahimzadeh*

aDepartment of Analytical Chemistry and Pollutants, Faculty of  Chemistry and Petroleum Sciences, Shahid Beheshti University, Tehran, Iran

∗ Corresponding author: Tel.: +98 21 29902891, fax: +98 21 22403041.

E-mail address: h-ebrahim@sbu.ac.ir (H. Ebrahimzadeh)

Table S.1. Operation conditions of CD-IMS for the determination of ATZ and AMT

| Parameters | Setting |
| --- | --- |
| Carrier gas flow (N2) | 500 mL/min |
| Drift gas flow (N2) | 700 mL/min |
| Drift field | 7 KV |
| Drift tube length | 11 cm |
| Shutter grid pulse | 200 µs |
| Corona voltage | 2.34 kV |
| Pulse voltage | 184 kV |
| Pulse width | 2.17 kV |
| Injection temperature | 200 °C |
| Cell oven temperature | 190 °C |

Fig S.1. Schematic illustration of TFME method using electrospun nanofibers of PVC/EVA/CS/Str as the sorbent for the extraction of ATZ and AMT in lettuce, tomato, and milk samples.

Fig S.2. The ATR-FT-IR spectra of PVC/EVA/CS/Str electrospun nanofibers.

Fig S.3. The formation of hydrogen bond in EVA.

Fig S.4. The XRD pattern spectra of PVC/EVA/CS/Str electrospun nanofibers.

Table S.2. Primary information for designing of CCD.

|  | Name | Unit | Low | High | -alpha | +alpha |
| --- | --- | --- | --- | --- | --- | --- |
| A | pH | --------- | 4.5 | 8.5 | 2.5 | 10.5 |
| B | Extraction time | min | 10 | 20 | 5 | 25 |
| C | Salt percent | %(w/v) | 10 | 20 | 5 | 25 |

Table S.3. Fit statistics of used CCD for optimization effective factors on adsorption of ATZ and Amt on PVC/EVA/CS/str electrospun nanofibers.

| Std. Dev. | 0.0488 |  | R² | 0.8863 |
| --- | --- | --- | --- | --- |
| Mean | 0.8489 |  | Adjusted R² | 0.7726 |
| C.V. % | 5.75 |  | Predicted R² | 0.2775 |
|  |  |  | Adeq Precision | 7.7937 |

Fig S.5. optimization of other effective factors on adsorption process by OAT, A: sorbent size, B: sorbent type, C: stirring rate.

Fig S.6. optimization of effective factors on desorption process by OAT, A: eluent type, B: eluent volume, C: desorption time.

Fig S.7. The reusability of PVC/EVA/CS/str electrospun nanofibers.