Supplementary Information

Conducting polymer/hydrogel hybrid free-standing electrodes for flexible supercapacitors capable of self-sensing working conditions: large-scale fabrication through facile and low-cost route

Madari Palliyalil Sidheekhaa, Aranhikkundan Shabeebaa, Lijin Rajana, Mohamed Shahin Thayyilb, Yahya A. Ismaila*

a Advanced Materials Research Center, Department of Chemistry, University of Calicut, Thenhipalam, Kerala - 673635, India

b Department of Physics, University of Calicut, Thenhipalam, Kerala - 673635, India

*Correspondence

Yahya A. Ismail

Department Of Chemistry, University of Calicut, Kerala, India- 673635

aiyahya123@gmail.com; aiyahya@uoc.ac.in

- Cs/PANI hybrid film

Fig. S1: photograph of fabricated CPF hybrid hygrogel film

- EDS analysis

Fig. S2: SEM-EDX spectra of Chitosan and CPF films

- Cyclic voltammograms at different scan rate

Fig. S3: (a,b and c) CVs obtained at different scan rates for CPF1, CPF2 and CPF3 films respectively and (c,d and f) variation peak current as a function of square root of scan rate for CPF1, CPF2 and CPF3 films respectively

- Chronopotentimetric responses during consecutive oxidation/reduction cycles

Fig. S4: (a) A representative square current waves applied to the CPF working electrode and (b) resulting chronopotentiometric responses

- CVs of CPF films at the scan rate of 5 mV s-1

Fig. S5: CVs at scam rate of 5 mV s-1

- Chronopotentiogram at different working current at constant charge for the device

Fig. S6: Second cycle of charge-discharge (oxidation-reduction) curve at different working (charging/discharging) currents by consuming constant charge of ±38 mC

- Mechanical properties of CPF films

Table S1: Tensile strength, Young’s Modulus and % elongation at break of CPF films

| Film | Tensile strength (MPa) | Young’s Modulus (MPa) | % Elongation at break |
| --- | --- | --- | --- |
| CPF1 | 9.82 | 2.32 | 8.12 |
| CPF2 | 8.22 | 1.99 | 7.08 |
| CPF3 | 6.64 | 1.85 | 6.42 |
| CPF4 | 5.84 | 1.56 | 5.86 |

- CV peaks of CPF film at scan rate 25 mV/s

Table S2: Anodic and cathodic peaks of CPF electrodes at the scan rate 25 mV/s

| Film | Anodic peaks (V) |  | Cathodic peaks (V) |  |
| --- | --- | --- | --- | --- |
|  | LE to ES | ES to PN | PN to ES | ES to LE |
| CPF1 | 0.27 | 0.54 | 0.43 | 0.059 |
| CPF2 | 0.28 | 0.54 | 0.42 | 0.11 |
| CPF3 | 0.28 | 0.59 | 0.48 | 0.19 |
| CPF4 | 0.29 | 0.57 | 0.45 | 0.13 |

LE- leucoemeraldine, ES- emeraldine salt, PN- pernigraniline

- EIS Fitting data of device

Table S2: The best fitting values of the equivalent circuit elements in Figure 13e for the impedance data of CPF device

| Parameters | Rs (Ω) | Q1 (CPE1) (S·sα1) | α1 | Rct1 (Ω) | Q2 (CPE2) (S·sα2) | α2 | Rct2 (Ω) | W (Ω. s-0.5) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Values | 19.6 | 0.00432 | 0.455 | 4.27 | 0.0348 | 0.784 | 46.5 | 0.0277 |