Supplementary Materials for

Quantum critical Tomonaga-Luttinger liquid in the anisotropic triangular antiferromagnet Ca3ReO5Cl2

S. Lee,1,* C. H. Lee,2,* C. Wang,3 H. Luetkens,3 and K.-Y. Choi4,†

1Center for Integrated Nanostructure Physics, Institute for Basic Science, Suwon 16419, Republic of Korea

2Department of Physics, Chung-Ang University, Seoul 06974, Republic of Korea

3Laboratory for Muon Spin Spectroscopy, Paul Scherrer Institute, 5232 Villigen, Switzerland

4Department of Physics, Sungkyunkwan University, Suwon 16419, Republic of Korea

* These authors contribute equally: S. Lee and C. H. Lee

† Correspondence to: choisky99@skku.edu

This PDF file includes:

Supplementary Figures 1 to 5

Supplementary Figure 1 (a) Representative 35Cl NMR spectra at T=4 K for the applied fields along the crystallographic b- and c-axis. (b) Temperature dependence of the full width at half maximum for six NMR signals in the applied field of μ0H=10.5 T//b. (c) Angular dependence of the field difference μ0Hc–μ0Hs between the central peaks (c for P3 and P4) and the satellite peaks (s for P1, P2, P5, and P6) at T=4 K. Note that θ=0° (90°) corresponds to the field direction of μ0H//b and μ0H//c. The solid curve is the angular dependence of the quadrupolar splitting calculated by a simple cylindrical electric field gradient for the nuclear spin I=3/2: Δν=μ0Hc–μ0Hs=νQ(3cos2θ-1), where νQ=e2qQ/2h and θ is the angle between the principal axis of the electric field gradient tensor and the applied field. The cylindrical electric field gradient model cannot reproduce the observed angular dependence of the quadrupolar splitting.

Supplementary Figure 2 (a) Temperature dependence of the Knight shift in a field of μ0H=10.5 T applied along the b-axis. (b) Plot of the nuclear magnetization recovery curves as a function of time at T=4 K. The solid lines indicate the fits using M∞-Mt2M∞=0.9exp-6tT1+0.1exp-tT1+G, where G is the baseline correction constant. The spin-lattice relaxation time T1 is evaluated to be 0.78 s and 0.86 s for the short (π/2=3 μs) and long (π/2=35 μs) pulses, respectively. (c) Temperature dependence of the spin-lattice relaxation rate 1/T1 at different fields. The dashed lines represent the power-law behavior 1/T1~T-n. (d) Clogston-Jaccarino plot of the Knight shift for P1 vs. the dc magnetic susceptibility χ. The dashed line indicates the linear fit in the temperature range of T=20–80 K, providing the hyperfine coupling constant of Ahf=46.21 mT/μB.

Supplementary Figure 3 (a) Representative ZF-μSR spectra at different temperatures. (b) LF-μSR spectra at T=1.6 K in various applied fields. The solid curves indicate the fittings of the data using a sum of two simple exponential functions as described in the main text. (c) Temperature dependence of the fast relaxation rate λf(T) in zero field. Below 5 K, λf(T) abruptly increases because the system approaches the antiferromagnetic ordering temperature TN=1.13 K. (d) Slow relaxation rate as a function of temperature λs(T) in zero field. λs(T) is nearly independent of temperature with the average value of λsavg(T)=0.0839 μs-1.

Supplementary Figure 4 LF dependence of the fast muon relaxation rate λf(T, HLF) at T=1.6 K. The solid, dashed, dotted, and dashed-dot curves denote the fits using 2D diffusive, 1D diffusive, ballistic models, and Redfield formula, respectively. The 1D diffusive and ballistic models yield λf(HLF)~HLF-1.0(1) and λf(HLF)~ln(130/HLF), respectively. The Redfield formula with Hloc=36(3) G and ν=1.9(4) MHz shows the deviation from the data in the intermediate field range of 10–100 G. The best description of λf(HLF) is obtained from the 2D diffusive model.

Supplementary Figure 5 LF dependence of the fast muon relaxation rate λs(T, HLF) at different temperatures. The solid curves represent the fits to the Redfield formula.