Supporting information

Pressure-induced phase separation for microstructural formation control in supercritical polymer solution: A promising solution enhancing mechanical properties of flash-spun filament

Jae-Hyung Wee 1†, Younghwan Bae1, Nam Pil Cho1,2, Moo Sung Kim3, Won Jun Lee2, Sang Young Yeo1*

1 Advanced Textile R&D Department, Korea Institute of Industrial Technology, 143 Hanggaulro, Sangnok-gu, Ansan-si, Gyeonggi- do, 15588, Republic of Korea

2Department of Fiber System Engineering, Dankook University, 152 Jukjeon-ro, Suji-gu, Yongin-si, Gyeonggi-do, 16890, Republic of Korea

3Department of Polymer Engineering, Graduate School, School of Polymer Science and Engineering & Alan G. MacDiarmid Energy Research Institute, Chonnam National University, 77 Yongbong-ro, Buk-gu, Gwangju 61186, Republic of Korea

* Corresponding author: miracle@kitech.re.kr (S. Y. Yeo)

Table S1. Thermal property parameters obtained by DSC curve at 20 ºC/min.

| Samples | Tm a) (°C) | Tc b) (°C) | ∆Hc c) (J/g) | Crystallinity d) (%) |
| --- | --- | --- | --- | --- |
| FSF-134 | 131.3 | 114.1 | 165.2 | 57.5% |
| FSF-113 | 133.2 | 115.1 | 173.7 | 60.5% |
| FSF-87 | 133.5 | 114.4 | 178.5 | 62.2% |
| FSF-76 | 133.3 | 115.2 | 189 | 65.8% |
| FSF-69 | 131.3 | 114.0 | 170.9 | 59.5% |
| FSF-65 | 130.7 | 113.4 | 167.5 | 58.3% |

*a) Tm: Melting temperature, b) Tc: crystallization temperature, c) ∆Hc: crystallization enthalpy, d) crystallinity calculated based on 100 % crystallization of HDPE (287.2 J/g).

Figure S1. Schematics of (a) lab-scale flash-spinning apparatus and (b) multi-stage nozzle with extended volume for pressure-induced phase separation (orifice diameter is 0.7 μm).

Fig. S2. Schematic of the high-pressure view cell system.